Adsorption (2014) 20:801–821 DOI 10.1007/s10450-014-9623-y
Enzyme immobilization by adsorption: a review
Teofil Jesionowski•Jakub Zdarta•
Barbara Krajewska
Received: 21 January 2014 / Revised: 14 May 2014 / Accepted: 18 June 2014 / Published online: 27 June 2014
©The Author(s) 2014. This article is published with open access at Springerlink.com
Abstract Endowed with unparalleled high catalytic activity and selectivity, enzymes offer enormous potential as catalysts in practical applications. These applications, however, are seriously hampered by enzymes’ low thermal and chemical stabilities. One way to improve these sta- bilities is the enzyme immobilization. Among various tested methods of this process that make use of different enzyme-carrier interactions, immobilization by adsorption on solid carriers has appeared most common. According to these findings, in this review we present a comparative analysis of the literature reports on the recent trends in the immobilization of the enzymes by adsorption. This thor- ough study was prepared in order to provide a deeper understanding of the process. Both carriers, carrier modi- fiers and procedures developed for effective adsorption of the enzymes are discussed. The review may thus be helpful in choosing the right adsorption scheme for a givenenzyme to achieve the improvement of its stability and activity for a specificapplication.
1 General overview
Low thermal stability, narrow pH range, effective activity in water environment and the loss of catalytic activity after one cycle have been the greatest obstacles in the use of the enzymes in the multiple practical processes (Liese and Hilterhaus2013; Gray et al.2013; DiCosimo et al.2013). However, the enormous catalytic potential offered by the enzymes for innumerable transformations, has stimulated intense studies aimed at the improvement of their proper- ties (Mateo et al.2007; Brady and Jordon2009;Fernandez- Lafuente2009; Garcia-Galan et al.2011; Cowan and Fernandez-Lafuente2011; Rodrigues et al.2013). Among several methods of this improvement that have been pro- posed, an immobilization of the enzymes is apparently most widely applied (Zhao2010; Rodrigues et al.2011; Hanefeld et al.2013). The term first appeared in the liter- ature at the beginning of twentieth century and referred to the enzymes bound directly to the carriers. At present this term has been extended to include both direct immobili- zations on the carriers and the immobilizations supported with the intermediate agents (Cao et al.2003; Hanefeld et al.2009).
An immobilization of the enzymes on the solid carriers can be achieved using a broad variety of chemical and physical methods (Cao2005; Sheldon2007; Sheldon and van Pelt2013). Among many methods proposed for the protein immobilization, the most important and useful is the immobilization by adsorption. Adsorption makes use of the physical interactions generated between the carrier and enzyme that include van der Waals forces, ionic interac- tions and hydrogen bonding. The binding are rather weak and, what is important, typically are does not change the native structure of the enzyme. This prevents the active sites of the enzyme from disturbing and allows theenzyme
Keywords Enzymes immobilization·Adsorption·
Carriers·Surface modifying agents·Applications
T. Jesionowski (&)·J. Zdarta
Faculty of Chemical Technology, Institute of Chemical Technology and Engineering, Poznan University of Technology,
M.Skłodowskiej-Curie2,60965Poznan´,Polande-mail:teofil.jesionowski@put.poznan.pl
B. Krajewska
Faculty of Chemistry, Jagiellonian University, Ingardena 3,30060Krako´w,Poland
13

802
Adsorption (2014) 20:801–821
general classification of typical carriers used for the enzyme adsorption is presented in Fig.2.
In general, the carriers used for the enzyme immobili- zation by adsorption can be divided into both organic and inorganic origin. The most common inorganic carriers are silicas, titania and hydroxyapatite. The organic carriers by contrast, include compounds of natural origin, such as chitin, chitosan, cellulose and alginate, also the synthetic compounds, mainly polymers. The advantage of these matrices is that they can be readily chemically modified tomatch conditions for a given enzyme and its application.
Another important advantage of the enzyme immobili- zation is that the immobilized enzymes may show prop- erties that can be exploited in the reactions performed in non-aqueous environments. Typically, the native enzymes are catalytically active in the aqueous media and they lose the activity in organic solvents. However, when immobi- lized, the enzymes may have their catalytic properties altered in a manner permitting them to preserve their activities in conditions other than aqueous. This is impor- tant for two reasons. One is that such enzymes can be used for the transformations of hydrophobic substrates that can only be performed in organic solvents (Carrea and Riva2000; Klibanov2001; Iyer and Ananthanarayan2008). The other one is that the immobilized enzymes may exhibit catalytic properties in organic solvents different from those in aqueous environments. This can be exploited in guiding the reactions toward the desired products. Excellent examples of such properties are lipases and esterases; in aqueous environments those enzymes catalyze the hydro- lysis of esters to alcohols, while in organic solvents they catalyze transesterifications of the same substrates (Kliba- nov2001). Additionally, along with the use of the specific organic solvents, the following properties can be achieved:
ENZYME
ENZYME
SURFACEMODIFIER
CARRIER
ENZYME
ENZYME
Fig. 1 Enzyme immobilization by adsorption
to retain its activity (Hernandez and Fernandez-Lafuente2011; Hwang and Gu2013). Notably, any carrier can be applied for enzyme adsorption, but not every enzyme can be immobilized on all carriers. The reason is that for the successful adsorption of the enzyme to occur, some certain conditions must be met, among which an enzyme-carrier affinity is most important. This is assured by the presence of the specific active groups on the carrier, which enable the generation of the enzyme–carrier interactions. How- ever, if absent, the interactions can be tuned by applying intermediate agents (carrier modifiers) (Fig.1).
A wide range of available compounds can be success- fully used as the enzyme carriers. The criteria of the choice suitable for a given enzyme and its application include: the cost, availability, stability (or reactivity if necessary) in specific conditions, and the type of reactor. The physico- chemical parameters of the carrier that should be taken into an account are: the surface area, particle size, pore struc- ture and type of functional groups present on the surface. A
Fig. 2 Carriers used for enzyme immobilization by adsorption
13
Chitin Chitosan Starch Alginate Collagen Carrageenan Cellulose Agar-Agar
Polyacrylamide Polyurethane Polypropylene Polystyrene Silicons
Ion-exchange resins
Epoxy resins
Natural
Synthetic
Silica Silica gel
Metal oxides Diatomaceous earth Hydroxyapatite Cordierite Porous glass
Inorganic
Organic

Soluble dextrans Poly(vinyl alcohol) Poly(oxyethylene glycol)
Insoluble

Soluble

Enzyme carriers

Adsorption (2014) 20:801–821
803
reaching 750 m2/g, pore radius from 7 to 10 nm and pore volume from 0.9 to 1.0 cm3/g. By contrast, in mesoporous silica MCM-41 (Mobil Composition of Matter), with hex- agonally ordered mesopores (Choma et al.2004; Weber et al.2010), the pore size is from 2 to 8 nm, which is controlled by adjusting the synthesis conditions and/or by applying surfactants with different chain lengths (pore sizes 2–5 nm) or expanders (pore sizes up to 8 nm) in their preparation.Theporevolumeinthissilicaiscloseto
1.0 cm3/g and its surface area exceeds 1,200 m2/g (Magner2013), which are features that classify this material as a carrier for the enzyme immobilization. FDU-12 (Fudan University Material) (Hartono et al.2010) is another mesoporous silica material with face-centered cubic structures of spherical mesopores and surface area of about 700 m2/g, pore size from 10 to 15 nm and pore volume from 0.6 to 0.7 cm3/g. This silica and other silica matrices (Falahti et al.2012) differing in pore size and structure, are also excellent carriers for enzyme immobilization. Like- wise, highly ordered mesoporous silicas with 2D and 3D structures and mesopores from 2 to about 30 nm, obtained by a surfactant and block copolymer templating, can be readily applied. The material of 3D structure is a better adsorbent and permits immobilization of a greater amount of the enzyme. The small particle of mesoporous silica (Chang et al.2011) was reported to have a surface area of 820 m2/g and a pore diameter varying from 2 to 5 nm, while the diameter of particles was close to 150 nm. This small particle mesoporous silica was compared with thelarge particle mesoporous silica (Chang et al.2011), which surface area was near 260 m2/g, pore diameter varied from20 to 40 nm and particle size reached 600 nm. It was found that the larger surface area and smaller particle diameter favoured an immobilization of a greater amount of the enzymes. CubicIa3dmesoporous silica nanoparticles (Falahati et al.2011) have the surface area of over 820 m2/ g, pore diameters of about 7 nm and pore volume greater than 1.5 cm3/g. To increase the surface area of the carrier available to the enzyme, the folded sheet mesoporous silica was proposed (Nara et al.2010). Such a configuration permits an immobilization of the greater amounts of the enzymes at only insubstantial growth of cost of the carrier production. Silicas of smaller surface areas obtained mainly in the processes of hydrolysis and condensation of tetraalkoxysilanes (Grabicka and Jaroniec2010; Fornera and Bauer2012; Zheng et al.2012) were also used for the enzymeimmobilization.
Othersilicacarrierswidelyusedfortheenzymeadsorption are silica gels (Bhattacharyya et al.2010; Lee et al.2010). Theyhaveverywelldevelopedporousstructuresandsurface areas, as well as high mechanical strength and thermal sta- bility.Thesizeofsilicagelparticlesvariesfrom70to150lmdependingonthetypeandtheporesizereaches250nm.
chemo-, regio- and enantioselectivity of the enzymes afterimmobilization may be customized for a specific purpose(Carrea and Riva2000; Klibanov2001), the reactions canbe reversed, their yield may be increased, and also thehomogeneous product may be obtained rather than a mix-ture of isomers or enantiomers. Importantly, it should notbe overlooked that the water, present in an organic solvent,even in trace amounts, may significantly alter the param-eters of the preparation obtained and may even affect thecourse of the entire process. Interestingly, organic solventsalso affect the stabilities of the immobilized enzymes. Thisis because the enzymes desorb from the carriers to theorganic solvents less readily than to the aqueous solutions.
Given the growing importance of immobilized enzymes as well as the complexity of their preparation, this review presents a thorough study on literature dealing with the immobilization of the enzymes by adsorption. Carriers utilized for the immobilization with and without the intermediate agents are reviewed, methods of adsorptionon different types of the carriers are compared, and examples of the immobilized enzymes employed as catalysts in practical applications both in aqueous and non-aqueous (organic solvents, surfactants, ionic liquids) media are discussed. The data taken from the literature are presented as a summary in Table1and discussed individually in the subsequent sections: Carriers in Sect.2, Surface modifiers in Sect.3, and Properties of immobilized enzymes in Sect.4.
2 Carriers used for immobilization of enzymes by adsorption
2.1 Inorganic carriers
Among many inorganic carriers used for immobilization of enzymes by adsorption, silicas are apparently those carri- ers, which have drawn most attention (Erhardt and Jor- dening2007; Magner2013; Hartmann and Kostrov2013). Silicas of different dispersive-morphological parameters and porous structures have been proposed. Arepresentative silica used for the enzyme immobilization on a large scale is mesoporous silica SBA-15 (Santa Barbara Amorphous) with hexagonal array of pores (Salis et al.2010; Thorn et al.2011). It is characterized by small pores, from 5 to about 30 nm in diameter and a hexagonal array of pores(Grudzien´etal.,2006;2007;HartmannandKostrov2013).Large volume of mesopores, close to 1.0 cm3/g and mi- cropores of about 0.8 cm3/g, and also a very well devel- oped surface area from 500 to 1400 m2/g [Hartmann and Kostrov2013] make this silica an excellent support for the enzyme immobilization. Another mesoporous silica MSU- H(YuandFang2013)hasthespecificsurfacearea
13

Table 1 Immobilization of enzymes by adsorption
Enzyme
Carrier
Carrier modifier
Research techniques
Examined properties and applications
Ref.
Alanine racemase fromGeobacillusstearothermophilus
a-Amylase fromBacillussubtilis
a-Amylase fromBacillusspecies
Folded-sheet mesoporous silica
–
Pore structure characterization
Catalytic properties; chemical, thermal and operational stability. Activity assay based on racemization ofL-alanine toD-alanine
Nara et al. (2010)
Mesoporous silica SBA-15
Mesoporous silica thin film
XRD, SEM, HR-TEM, pore
structure characterization
TEM, FE-SEM, XRS, XRD,
EEP, spectrophotometric measurements
Bradford method
Optimization of immobilization conditions: effects of pore size, pH and time of immobilization
Activity and stability versus pH and temperature. Activity assay based on hydrolysis of starch
Ajitha et al. (2010)
Bellino et al. (2010)
Amylase fromAspergilluscarbonarius
Silica gel
Glutaraldehyde
Optimization of immobilization conditions: glutaraldehyde concentration, pH and temperature. Thermal and chemical stability
Activity; thermal, chemical and storage stability, reuse. Application in hydration and sequestration of CO2
Nwagu et al. (2011)
XRD, FE-SEM, FTIR,29Si CP
MAS NMR, Bradford method, pore structure
HPLC
Carbonic anhydrase from bovine
Mesoporous silica SBA-15
3-Aminopropyltriethoxysilane
Vinoba et al. (2012)
Carbonyl reductase from
Georichum candidum
Silica gel
–
Comparison of immobilization methods. Stability. Adsorption efficiency. Activity assay based on conversion of
1-acetonaphthoneto(S)(–)-1-(10-naphthyl)ethanol
Carrier and modifier characteristics. Activity and stability. Amount of adsorbed enzyme versus modifying agent. Application in bioadsorption, biomolecule separation and in pharmaceutical industry
Activity; thermal and storage stability, Optimization of immobilization parameters. Application in hydrolysis of carboxymethylcellulose
Activity and stability. Application in hydrolysis of cellulose to glucose in water. Elaboration of universal immobilization method
Bhattacharyya et al. (2010)
XPS, SAXS, TEM,13C CP
MAS NMR, zeta potential, pore structure, spectrophotometry
EA, SEM, FTIR
Carboxymethyl cellulase from
Trichoderma reesei
Large pore silica FDU- 12
3-Aminopropyltriethoxysilane;3-Mercaptopropyl-, Phenyl- and Vinyltrimethoxysilanes
Hartono et al. (2010)
Cellulase fromTrichodermaviride
Silica grafted with polyamidoamine dendrymers
Mesoporous silica
–
Wang et al. (2013)
Cellulase fromTrichodermareesei
XRD, SEM, TEM, UV–Vis,
29Si CP MAS NMR,13C CP
MAS NMR, pore structure characterization
FTIR, XRD, SEM, TEM,
fluorescent spectroscopy, pore structure
HPLC, spectrophotometric measurements
Chang et al. (2011)
Chloroperoxidase from
Caldariomyces fumago
Mesoporous silica SBA-15
Activity assay based on oxidation of 4,6-dimethyl dibenzthiophene. Carrier characteristics. Kinetic parameters; catalytic activity, storage and thermal stability
Kinetic parameters; thermal stability, reuse. Influence of organic solvent and inhibitory agents. Activity assay based on reaction of chlorophyll
Applications in digestion of proteins. Catalytic activity and product stability
Activity assay based on transestrification of methyl hydroxycinnamate with butanol to butyl hydroxycinnamate. Thermal and chemical stability
Applications in electrodes as sensors of glucose detection. Catalytic properties and stability versus various immobilization methods
Montiel et al. (2007)
Chlorophyllase from
Phaedactylum tricornutum
Silica gel, cellulose
Diethylaminoethyl
Karboune et al. (2005)
Chymotrypsin
Aptamer-silica beads
Glutaraldehyde
HPLC, spectrophotometric measurements
HPLC, Bradford method
Xiao et al. (2012)
Thorn et al. (2011)
Feruloyl esterase (used as Depol 740L)
Mesoporous silica SBA-15
–
Glucose oxidase from
Aspergillus niger
Rod-like and vesicle- like mesoporous silica
3-Aminopropyltrimethoxysilane
HR-TEM, FTIR, FE-SEM,
ampero- and voltometric measurements, pore structure
Zhou et al. (2011)
804
Adsorption (2014) 20:801–821
13

Table 1 continued
Enzyme
Carrier
Carrier modifier
Research techniques
Examined properties and applications
Ref.
Glucose oxidase from
Aspergillus niger
Peroxidase from horseradish
Silica
Second generation dendronized polymer, avidin–biotin system
spectrophotometric measurements
Application in reaction of b-D-glucose to glucono-d-lactone and H2O2
Utilization in oxidation of o-phenylenediamine to 2,3- diaminophenazine
Activity assay based on amount of H2O2formed in hydrolysis of b-D-glucose. Elaboration of the effective immobilization method. Immobilization efficiency and catalytic activity versus pH, temperature and storage time
Fornera and Bauer (2012)
Glucose oxidase from
Aspergillus niger
Silica gel 100
Acrylonitrile copolymers
-vinyl pyridine
-vinyl
imidazole
-N,N-dimethyl aminoethyl methacrylate
Lowry method, spectrophoto- metric measurements
Godjevargova et al. (2006)
1H NMR,13C NMR,
spectrophotometric measurements
XRD, TG/DSC, pore structure characterization
Laccase fromAspergillus
Silica
Glutaraldehyde
Effect of the ionic liquid. Optimum pH and enzyme concentration. Kinetic parameters
Tavares et al. (2013)
Laccase fromTrametesversicolor
Mesoporous silica SBA-15
–
Activity assay based on oxidation of phenol and 4-aminoantipyrine. Use in biodegradation of naphthalene. Adsorption efficiency.
Activity versus catalytic cycles
Improvement of thermal and chemical stability. Catalytic activity, thermal and chemical stability
Application in estrification of linoleic acid with ethanol in organic solvent. Catalytic activity versus different immobilization methods and reuse
Catalytic activity. Activity assay based on hydrolysis of p-nitrophenyl palmitate to p-nitrophenol. Application in estrification of phytosterols from oleic or linoleic acid
Catalytic activity and amount of enzyme adsorbed versus surface modifier. Activity assay based on hydrolysis of p-nitrophenyl butyrate in DMF. Application in estrification and hydrolysis in organic solvents
Activity assay based on hydrolysis of acetate 4-nitrophenolate to 4-nitrophenol. Effect of pH and type of enzyme on amount of enzyme adsorbed
Activity assay based on hydrolysis of triacetin. Elaboration of fast, universal and effective immobilization. Activity and stability versus temperature, storage time, pH and reuse
Bautista et al. (2010)
Lipase fromCandida rugosa
Vesicular silica
FTIR, FE-SEM, TEM, pore
structure, Bradford method FTIR, XRD, TG/DTA, pore
structure, Bradford method
Wu et al. (2012)
Yu et al. (2013)
Lipase fromCandida rugosa
Mesoporous silica MSU-H
Glutaraldehyde
Lipase fromCandida rugosa
Silanized silica
n-Octyltriethoxysilane,3-Mercaptopropyl- triethoxysilane
Multi-walled carbon naotubes
–
Zheng et al. (2012)
Lipase from:Candida rugosaand antarctica, Thermomyces lanuginosusandMucorjavanicus
Lipase fromMucor mieheiand
Rhizopus oryzae
Silica sol–gel
Lee et al. (2010)
Mesoporous silica
–
SEM, TEM, UV–Vis, SAXS,
pore structure
Gustafsson
et al. (2012)
SAXRD, FTIR, SEM, TG,13C
CP MAS NMR, pore structure characterization
Lipase from porcine pancreas
Mesoporous silica SBA-15
Ionic liquid
Yang et al. (2013)
Adsorption (2014) 20:801–821
805
13

Table 1 continued
Enzyme
Carrier
Carrier modifier
Research techniques
Examined properties and applications
Ref.
Lipase fromPseudomonasfluorescens
Lipase B fromCandidaantarctica
Mesoporous silica SBA-15
Fumed silica
–
XRD, TEM, HPLC, pore
structure, Bradford method
HPLC, XRD
Utilization in biodiesel production. Carrier characteristics. Catalytic activity decrease after reuse
Activity assay based on separation of (R,S)-1-phenyl-ethanol and vinyl acetate to R-1-phenylethyl acetate and (S)-1-phenylethanol. Activity and stability vs solvent, water content, temperature and immobilization time. Utilization in enantioselective reactions in hexane
Carrier characterization. Optimization of immobilization. Activity and adsorption versus carrier. Activity assay based on reaction of p-nitrophenoxy-dodecanoic acid to p-nitrophenolate and on conversion of n-octane
Elaboration of universal enzyme immobilization method. Catalytic activity veruss storage time
Salis et al. (2010)
Kramer et al. (2010)
P450 BM-3 monooxygenase from heme domain
Mesoporous silica SBA-15 and MCM- 41
XRD, pore structure characterization, spectrophotometric measurements
SEM, XRD, TG, pore
structure, spectrophotometric measurements
FTIR, XRD, TG, EA, TEM,
pore structure, zeta potential
Weber et al. (2010)
Peroxidase from horseradish
Mesoporous silica composite with polypirol
Kwon et al. (2012)
Superoxide dismutase from bovine erythrocytes
Mesoporous silica nanoparticles
Aminosilane
Immobilization efficiency versus surface modifiers and enzyme concentration. Thermal and chemical stability. Influence of denaturating agents. Industrial uses
Catalytic activity. Elution rate from carrier. Elaboration and optimization of immobilization method
Falahti et al. (2012)
Superoxide dismutase from bovine erythrocytes
Mesoporous silica nanoparticles
3-Aminopropyltriethoxysilane
XRD, FTIR, CD, DSC, TG,
pore structure, spectrophotom
TEM, EDX, VSM, SEM, HPLC
Falahati et al. (2011)
Endo-glucanase,Exo- glucanase, b-glucosidase
Gold nanoparticles; gold-doped magnetic silica nanoparticles
Gold nanotubes
3-Mercaptopropyltriethoxysilane
Chemical, thermal and storage stability. Applications in hydrolytic degradation of cellulose
Cho et al. (2012)
Glucose oxidase from
Aspergillus niger
Glutaraldehyde
DSM, XPS, amperometric measurements
Utilization as an enzymatic biosensor to glucose detection in physiological fluids
Delvaux and Demoustier-Champagne (2003)
Yu and Ju (2002)
Reshmi et al. (2007)
Peroxidase from horseradish
Titania sol–gel film
–
SEM, voltometric measurements
Application in biosensors to H2O2detection. Influence of pH on catalytic activity. Storage time stability
Application and activity assay based on starch hydrolysis. Kinetic parameters. Activity and stability vs buffer, pH, temperature and immobilization time
Effect of surface modifier, reuse and storage time on catalytic activity and stability. Use in resolution of (R,S)-ibuprofen and (R,S)-1-phenylethanol
a-Amylase fromBacillussubtilis
Zirconia
XRD, IR, pore structure characterization
Lipase fromCandida rugosa
Zirconium dioxide nanoparticles
Eruic acid, Tween 85
TEM, FTIR, EA, TG
Chen et al. (2008)
806
Adsorption (2014) 20:801–821
13

Table 1 continued
Enzyme
Carrier
Carrier modifier
Research techniques
Examined properties and applications
Ref.
Trypsin
Layered c-zirconium phosphate
–
XRD, UV–Vis
Optimization of pH and temperature conditions. Chemical and thermal stability. Activity assay based on hydrolysis of
N-benzoyl-p-nitroanilide
Activity and stability versus pH and buffer. Kinetic parameters. Application in starch hydrolysis to low molecular weight compounds
Kinetic parameters; Activity and stability versus pH and temperature. Optimization of immobilization. Activity assay based on reaction of p-nitrophenyl acetate. Application in carbonation process in production of CaCO3from CO2
Activity assay based on hydrolysis of sucrose. Amount of adsorbed enzyme on various carriers. Effects of pH, temperature, inhibitors. Activity and kinetic parameters versus storage time and reuse
Geng et al. (2003)
a-Amylase fromBacillussubtilis
Alumina
XRD, IR, pore structure, spectrophotometric measurements
XRD, FTIR, GC, SEM, TEM,
TCD, pore structure characterization
Reshmi et al. (2006)
Carbonic anhydrase
Mesoporous aluminosilicates
Wanjari et al. (2012)
Dextransucrase from
Leuconostoc mesenteroides
Hydroxyapatite Calcium alginate Alumina gel
Calcium phosphate gel Bentonite Hydroxyapatite Streamline DEAE Silica
Hydroxyapatite
Spectrophotometric measurements
Gupta and Prabhu (1995)
Endodextranase from
Chaetomium erraticum
Bradford method
Kinetic parameters, adsorption efficiency. Optimization of pH of immobilization process. Application in synthesis of isomaltose using dextransucrase
Erhardt and Jordening (2007)
Fructosyl transferase from
Steptococus mutans
–
Influence of carrier structure on adsorption efficiency. Activity assay based on sucrose conversion to fructanes insoluble in ethanol
Bronshyteynand Steinberg (2002)
Liu et al. (2013)
Marzadori
et al. (1998)
Zhai et al. (2010)
de Lathouder et al. (2008)
Lyase hydroperoxide from
Amaranthus tricolor
Urease fromCanavaliaensiformis
a-Amylase, Urease
Ceramic hydroxyapatite
Hydroxyapatite
–
Spectrophotometric measurements
–
Activity versus temperature and pH. Kinetic parameters; thermal and chemical stability. Use in food industry
Kinetic parameters; thermal, chemical and storage stability
Halloysite nanotubes
TEM, XRD, FTIR, pore structure characterization
SEM, FTIR, TG/DTA,
spectrophotometric measurements
Bradford method, pore structure characterization
Activity assay based on starch hydrolysis. Thermal and storage stability, reuse and catalytic activity
Activity assay based on hydrolysis of o-nitrophenyl-b- galactopyranoside. Optimization of immobilization. Catalytic activity, reuse and adsorption efficiency
Carrier adsorption capacity, immobilization efficiency. Activity vs reuse and temperature. Utilization in esterification of fatty acids and sugars (lactose esters)
Application in electrode as a sensor for detection of low levels of glucose
b-Galactosidase from
Aspergillus oryzae
Cordierite, Acicular mullite
3-Aminopropyltriethoxysilane;Glutaraldehyde
Lipase fromCandida rugosa
Mica
Glutaraldehyde
Zaidan et al. (2012)
Glucose oxidase
Pt nanoparticles/ graphene sheets/ chitosan film
Chitosan
–
TEM, amperometric and voltometric measurements
Wu et al. (2009)
Hexokinase from bakers yeast
Polystyrene
DLS, TEM, zeta potential, pore structure, spectrophotom
SEM, FTIR, AFM, EDAX
Activity assay based on reduction of NADP? to NADPH. Carrier characteristic. Activity on storage
Effects of pH and temperature on catalytic efficiency. Use in bioremediation of hazardous materials
Castro et al. (2007)
Bayramoglu et al.(2012)
Laccase fromTramatesversicolor
Chitosan membrane with epichlorohydrin
Itaconic acid, itaconic acid and Cu(II)
Adsorption (2014) 20:801–821
807
13

Table 1 continued
Enzyme
Carrier
Carrier modifier
Research techniques
Examined properties and applications
Ref.
Lipase fromCandida rugosa
Chitosan beads
–
TLC, Bradford metod
Activity assay based on transestrification of cooking oil. Application in transestrification
Application in sucrose conversion to isomaltulose–sucrose replacement in food industry
Nasratun et al. (2010)
Kawaguti et al. (2011)
Cells fromErwiniasp.D12
Calcium alginate; gelatin transglutaminase
Cellulose acetate membranes
spectrophotometric measurements
b-Galactosidase from
Kluyveromyces lactis
Oxygen plasma
HPLC, Bradford metod
Kinetic parameters. Optimization of temperature and pH. Activity and stability on reuse. Activity assay based on conversion of lactose to galactooligosaccharides. Application in food industry
Activityassaybasedonoxidationof2,20-anizo-bis-(3-ethylbenzothiazoline-6-sulfonate) and L-3-(3,4- dihydroxyphenyl)alanine. Kinetic parameters; catalytic activity, thermal, chemical stability and immobilization efficiency
Activity assay based on hydrolysis of p-nitrophenyldodecanoate. Catalytic properties. Influence of reuse on stability and catalytic activity
Gulec (2013)
Laccase fromCerrenaunicolor, Tyrosinase
Cellulose acetate disc membranes, poly(amide) disc membranes
Plasma polymerization, glutaraldehyde
ATR-FTIR, UV–Vis
Labus et al. (2012)
Allyl
alcohol
Allyl-
amine
Acrylic acid
Lipase fromCandida rugosa
Ultrathin film of cellulose acetate and propionate, and of acetate butyrate
Poly(o-toluidine)
–
AFM, contact angle, spectrophotometric measurements
Kosaka et al. (2007)
Amyloglucosidase from
Rhizopus
Spectrophotometric measurements
Optimization of immobilization. Carrier characteristics. Activity. Storage, thermal and chemical stability, reuse. Activity assay based on starch hydrolysis. Utilized for starch hydrolysis
Removal of CO2from gases. Effect of water content on carrier structure. Catalytic activity. Activity versus temperature and organic solvent. Amount of enzyme adsorbed versus unmodified and modified carrier
Ashly andMohanan(2010)
Zhang et al. (2009)
Carbonic anhydrase from bovine
Poly(acrylic acid-co- acrylamide)/ hydrotalcite nanocomposite hydrogels
Cationic resin Amberlite IR-120H
Cryo-SEM, FTIR, TEM,
fluorescence microscopy
Laccase fromTrametesversicolor
Glutaraldehyde
SEM, spectrophotometric measurements
Kinetic parameters; catalytic activity, thermal, chemical and storage stability. Optimization of immobilization method. Activity assay based on oxidation of ABTS
Catalytic activity. Optimization of immobilization conditions. Stabilities and reuse. Application in production of diacylglycerols by glycerolysis of soybean oil
Effect of metal ions and enzyme concentration on catalytic properties. Storage stability. Activity assay based on estrification of ferulic acid with ethanol to ethyl ferulate in DMSO
Effect of the matrix on immobilization. Catalytic activity. Utilization in vitamin E (tocopherol) transestrification with vinyl acetate to 2-methyl-2-butyl
Spinelli et al. (2012)
Lacitase ultra
Macroporous resin
–
SEM, HPLC, TLC, GC–MS
Liu et al. (2012a,b)
Commercial lipase
Celite 545
Glutaraldehyde
GLC
Kumar and Kanwar (2011)
Lipase B fromCandidaantarctica
Ion exchange resin Lewatit
Polymer (Purasorb)
Polypropylene (Accurel EP100)
–
HPLC–MS, SEM, pore structure characterization
Torres et al. (2008)
808
Adsorption (2014) 20:801–821
13

Table 1 continued
Enzyme
Carrier
Carrier modifier
Research techniques
Examined properties and applications
Ref.
Lipase fromCandida rugosa
Poly(N-methylolacrylamide)
Bradford method
Optimization of immobilization. Effect of temperature, pH, storage and reuse on activity and stability. Activity assay based on butyl butyrate synthesis (in organic solvents) or hydrolysis of olive oil (in aqueous solvent)
Immobilization efficiency, catalytic activity, thermal and chemical stability. Optimization of immobilization conditions
Effects from carriers and lipases on catalytic activity. Activity assay based on hydrolysis of olive oil, estrification of butyric acid with butanol and transestrification of babassu oil.
Application in biodiesel production
Utilization in biodiesel production. Stability in reactor. Influence of amount of adsorbed enzyme, temperature, immobilization time and water content on catalytic activity
Influence of water content, substrate concentration and temperature on activity. Storage stability. Activity assay based on hydrolysis of tributyrin to fatty acids
Catalytic activity and storage stability. Utilization in enantioselective transestrification acylation of b-hydroxy esters with various aryl groups and enantioselective transestrification of 1-phenyl methane
Thermal, chemical and storage stability on various carriers. Optimization of enzyme immobilization process. Activity assay based on gum arabic reaction
Catalytic activity, storage stability. Utilization in acidolysis of tuna oil and caprylic acid to triacyloglycerols
Santos et al. (2007)
Lipase fromPenicilliumcamembertii(Lipase G)
Lipase fromP.antarctica, T.lanuginosus 1,T. lanuginosus2,P. fluorescens,andG.thermocatenulatus
Lipase fromPseudomonascepacia
MANAE-agarose, Epoxy-SiO2-PVA
Small/largepolyhydroxybutyratebeads
Glutaraldehyde
Mendes et al. (2012)
Mendes et al. (2011)
–
GC, Bradford method
Polyacrylonitrile fibers
Bradford method
Sakai et al. (2010)
Lipase from porcine pancreas
Cross-linked polivinyl alcohol
GC
Ozturk and Kilinc (2010)
Brem et al. (2011)
Lipase ,,powder’’ 20 AK from
Pseudomonas fluorescens
Celite
Spectrophotometric measurements
Lipase (Pf2001) from
Pyrococcus furiosus
Hydrophobicitycarriers
Spectrophotometric measurements
Branco et al. (2010)
Lipase fromRhizopus delemar, Patalase 20000L fromMucormiehei
Nattokinase fromBacillussubtilis
Accurel MP1000
HPLC
Hita et al. (2009)
Polyhydroxybutyratenanoparticles
TEM, FTIR
Catalytic activity, thermal and chemical stability. Optimization of immobilization and elaboration of universal immobilization method
Influence of glucose and xylose on catalytic activity. Amount of enzyme adsorbed vs carrier. Thermal and chemical stability. Utilization in hydrolysis of short xylooligomers. Activity assay based on hydrolysis of p-nitrophenyl-b-D-xylopyranoside
Deepak et al. (2009)
b-Xylosidase fromAspergillusnigerUSP-67
PEI-SepharoseDEAE-SepharoseQ-Sepharose
CM-Sepharose MANAE-agaroseSulphopropylsepharosePumice particles Amberlite XAD-2000 Polystyrene foam
Sand
Amberlite XAD-7 LentiKats
–
MS, Bradford method
Benassi et al. (2013)
Cells fromPleurotus ostreatus
GC–MS, FTIR
Amount of enzyme adsorbed versus used carrier. Utilization in the biodegradation of fluorene
Akdogan and Pazarlioglu (2011)
Cells fromRhodococcus equiA4
HPLC
Application in biotransformation of nitrile derivatives
Kubac et al. (2006)
Adsorption (2014) 20:801–821
809
13

Table 1 continued
Enzyme
Carrier
Carrier modifier
Research techniques
Examined properties and applications
Ref.
Cycloisomalto-oligosaccharideglucanotransferase
Porous hollow-fiber membranes
Glicid methacrylate, diethyloamine
–
Amount of enzyme adsorbed versus catalytic activity. Application in dextran production from cycloisomaltooligosaccharides
Influence of numbers of adsorbed enzyme layers on catalytic activity. Activity assay based on estrification of olive oil with poly(vinyl) alcohol
Application in protein digestion
Kawakita et al. (2002)
Lipase fromThermomyceslanuginosus
Cotton flannel cloth
Polyethyleneimine
Karimpil et al. (2012)
Trypsin
Nylon membranes
Poly(styrene sulfonate)
MALDI MS
Xu et al. (2010)
Tuzmen et al. (2012)
Catalase
Magnetic poly(acrylamide- allylglycydyl ether) cryogels
Magnetic nanoparticles
–
SEM, FTIR
Influence of pH, temperature and ionic strength on activity. Kinetic parameters and storage stability. Optimization of immobilization process
Glycolate oxidase from
Medicago falcata
–
SEM, TEM, FTIR
Kinetic parameters; catalytic activity, storage, thermal and chemical stability reuse. Utilization in catalytic oxidization of glycolic acid to glyoxylic acid
Catalytic activity, amount of enzyme adsorbed. Activity assaybasedonhydrolysisof2,20-azinobis(3-ethylbenzthiazolin-6-sulfonate). Activity versus temperature, pH, reuse
Zhu et al. (2009)
Laccase fromTrametesversicolor
Magnetic mesoporous silica spheres
SAXS, VSM WAXS, SEM, TEM,
UV–Vis, pore structure, zeta potential, spectrophoto-metric measurements,
FTIR, SEM, XRD, pore
characterization, Bradford method
Pore structure characterization
Zhu et al.(2007)
Lipase fromBurkholderia
Magnetic nanoparticles Fe3O4–SiO2
[3-(Trimethoxysilyl) propyl] octadecyl dimethyl ammonium chloride
–
Carrier characteristics. Kinetic parameters. Application in transesterification of olive oil with methanol in biodiesel production
Activity and stability. Influence of water and methanol content on transestrification. Biodiesel production
Carrier characteristics. Activity. Optimization. Activity assay based on transestrification of soya oil with methanol.
Application in biodiesel production
Catalytic activity. Chemical and storage stability. Activity assay based on reaction of benzyl-N-(2-hydroxyethyl)-carbamate ethnolamine to benzyl-N-(2-hydroxyethyl)-carbamate glycine
Activity assay based on reaction of N-glutaryl-L-phenylalanine- p-nitroanilide.
Activity assay based on reaction of but-2-one with NADH as cofactor
Tran et al. (2012)
Lipase fromBrukholderia
Hydrophobic magnetic particles
Magnetic chitosan microspheres
Liu et al. (2012a,b)
Xie and Wang (2012)
Lipase fromCandida rugosa
Glutaraldehyde
TEM, FTIR, XRD
Chloroperoxidase from
Caldariomyces fumago
Agarose gel
Monoaminoethyl-N-aminoethyl
spectrophotometric measurements
Pesic et al. (2012)
a-Chymotrypsin from bovine pancreas
Yeast alcohol dehydrogenase fromSaccharomycescerevisiae
Glucose dehydrogenase fromGluconobacter cerinuscerevisiae
Reverse micellar from different substrates
Glutaraldehyde
Spectrophotometric measurements, Raman spectroscopy
Thudi et al. (2012)
Activity assay based on glucose and NADP concentration
810
Adsorption (2014) 20:801–821
13

Adsorption (2014) 20:801–821
811
Other types of silicas used for the enzyme immobili- zation are vesicular silica and fumed silica. Vesicularsilica (Zhou et al.2011; Wu et al.2012) has pores of a diameter ranging from 15 to 20 nm, a pore volume from 0.6to
1.4 cm3/g and surface area reaching 360 m2/g, while fumed silica (Kramer et al.2010) has particles of a diameter from 7 to 50 nm and a surface area of 255 m2/g. These silicas have well-developed surface areas, small particles and high mechanical strength, which make them attractivealternativestotheothersilicasdescribed.
In order to enhance the affinity of the enzymes to sili- cas, the modifications of the matrices with polymers were proposed. The modifications consist in mixing silicas with polymers or coating them with polymers (Kwon et al.2012). One group of polymers are polyamidoamine den- drimers (Wang et al.2013). These are highly branched complex compounds, which due to the presence of amino groups in their structure, facilitate the development of the enzyme-carrier bonds, thereby giving rise to a more effective immobilization. For instance, it was observed that with an increasing content of the dendrimer on the silica surface, the amount of immobilized enzyme increased from 32 mg/g to almost 87 mg/g after a full modification of the silica. Polyamidoamine dendrimers were reported to enhance the affinity to cellulases, a group of enzymes catalysing the decomposition of cellulose by cleaving b-1,4-glycoside bonds. Importantly, the enzymes immobilized on polyamidoamine dendrimers modified- silicas retained over 80 % of their activity after three full catalytic cycles. A similar effect was reported for a mes- oporous silica-polypyrrole composite. The effect was ascribed to the presence of hydroxyl groups inpolypyrrole. Another group of polymers applied for silica modifications are aptamers (Xiao et al.2012). These are short oligonu- cleotide chains (DNA or RNA fragments) able to form specificbondswiththecarrierandthebiocatalyst.
The noble metal applied as a carrier for the enzyme immobilization is gold. The preparations made on thebasis of gold are used mainly in the electrodes mounted in bio- sensors (Delvaux and Demoustier-Champagne2003), but they can also be employed in biodegradation of cellulose (Cho et al.2012). Gold is hardly soluble but easily mal- leable so its form can be well managed. For the enzyme adsorption, it is used in the form of nanoparticles, gold- doped magnetic silica nanoparticles (Cho et al.2012), and nanotubes (Delvaux and Demoustier-Champagne2003).
Another inorganic carrier employed for the enzyme immobilization is a titania sol–gel film (Yu and Ju2002). Titanium dioxide is a white solid of high melting point and good adsorption parameters.
Zirconia, a white crystalline solid with a high melting point and high chemical resistance, is also an attractive for the enzyme immobilization, where it is used in the form of
13
Table 1 continued
Enzyme
Carrier
Carrier modifier
Research techniques
Examined properties and applications
Ref.
Lipase fromThermomyceslanuginosus
Olive pomace powder
–
SEM, spectrophotometric measurements, Bradford method
FTIR, SEM, spectrophoto-metric measurements
Optimization of immobilization. Catalytic activity, thermal and chemical stability. Activity in reuse. Activity assay based on hydrolysis of p-nitrophenyl palmitate.
Kinetic parameters; catalytic activity, pH, temperature and enzyme concentration. Activity assay based on dopachrome formation fromL-DOPA
Yucel (2012)
Polyphenol oxidase from
Solanum tuberosum
Mesoporous activated carbon matrices MAC 200 and MAC 400
Artificial oil bodies
Kennedy et al. (2007)
Xylanase fromNeocallimastixpatriciarium
–
Activity assay based on hydrolysis of oat spelt xylan. Catalytic activity, thermal and chemical stability. Activity in reuse
Hung et al. (2008)

812
Adsorption (2014) 20:801–821
nanoparticles (Chen et al.2008), layered c-zirconium phosphate (Geng et al.2003) and as pure zirconium (Reshmi et al.2007).
In addition to the above-mentioned materials, also alu-mina gel (Gupta and Prabhu1995) and aluminium (Reshmiet al.2006) were tested as the enzyme carriers. Aluminiumis a common, malleable and plastic metal. Its derivativesare mesoporous aluminosilicates (Wanjari et al.2012), wellcharacterized (Jaroniec and Fulvio2013), which are a classof compounds made of aluminium, silicon and oxygen.They can be of either natural (zeolites) or synthetic origin.Some enzymes were also reported to be immobilized oncordierite and mullite (de Lathouder et al.2008). Theformer is a rare mineral belonging to the group of silicates,whereas the latter, a mineral related to aluminosilicates instructure and composition and it was used in the immobi-
lization in the form of acicular mullite.
Other minerals reported as the enzyme carriers are halloysite (Zhai et al.2010) and mica (Zaidan et al.2012). Mica is a multi-element mineral of a complex chemical composition that includes mainly aluminium, silicon, cal- cium, sodium and potassium, and in smaller amounts, lithium, magnesium, iron and manganese. The benefits offered by mica are its high thermal and chemical resistance.
Hydroxyapatite is another mineral used as a carrier for the immobilization of enzymes by adsorption (Fargues et al.1998; Marzadori et al.1998; Bronshyteyn and Steinberg2002). Built of calcium, phosphorus, oxygen and hydrogen, hydroxyapatite is easily available; it occurs in nature and can also be chemically synthesized. Being a component of bones, hydroxyapatite shows high biocom- patibility. It also displays high resistance to a wide range of reaction conditions. Its important advantage is the ability to bind practically all enzymes, where it is typically used as a powdered solid or as ceramic hydroxyapatite (Liu et al.2013).
Also bentonite was reported to be an enzyme carrier with high protein adsorption capacity (Erhardt and Jor- dening2007). Bentonite does not dissolve in waterbut readily swells, which is why bentonite-supported enzymes can be used in waterenvironments.
Useful as a carrier in the enzyme immobilization also appeared to be a mesoporous activated carbon (Kennedy et al.2007) of different pore sizes, such as MAC 200 andMAC4000.
Chitosan is a nontoxic, biocompatible and gel-forming cationic compound that can readily be prepared in different geometrical configurations, such as membranes, beads, nanoparticles, fibers, hollow fibers or sponges (Krajewska2005). It can also be applied in the microcrystalline form (Castro et al.2007). The special advantage of chitosan is that when dissolved in acidic solutions, it bears multiple positive charges on –NH3?groups along its linear chains. This feature allows it to readily develop electrostatic interactions with molecules containing negatively charged groups (Alatorre-Meda et al.2009; Krajewska et al.2011,2013a,b). Another adavantage of chitosan is that it can easily be chemically modified, which is possible due to the presence of modifiable functional groups (–NH2and –OH) on chitosan chains (Honarkar and Barikani2009).
A common organic compound used as an enzymecarrier is calcium alginate [Gupta and Prabhu1995]. Alginate is an anionic polysaccharide that offers attractive gel-form- ing, concentrating and stabilizing properties. Commercial varieties of alginate are extracted from seaweeds, including the kelpMacrocystis pyrifera,Ascophyllum nodosum, and various types of algae fromPhaeophyceaefamily. In additiontoitspureform,itcanalsobeusedadmixtured,
e.g. with gelatin and transglutaminase (Kawaguti et al.2011). It easily forms spherical particles with a well- developed surface area that endow it with good adsorption properties.
Alternatively used, organic carrier is cellulose. This is a polysaccharide of natural origin, made of glucose mole- cules. On the industrial scale, cellulose is obtained from wood. It is frequently used in the form of colourless cel- lulose acetate. It is a thermoplastic but hardly combustible polymer, insoluble in water. Different structures made of cellulose acetate are utilized, e.g. cellulose acetate mem- branes (Gulec2013), cellulose acetate disc membranes (Labus et al.2012) or ultrathin film of celluloseadmixtured with acetate propionate and acetate butyrate (Kosaka et al.2007).
Agarose gel (Pesic et al.2012), a polysaccharide poly- mer,typicallyappliedforseparationofnucleicacids,isalso used for enzyme immobilization, which is due to its mor- phological structure and beneficial adsorptionproperties.
In addition to natural polymers, synthetic polymers form a large and varied group of the enzyme carriers (Kumarand Kanwar2011; Brem et al.2011). Effectively, any poly- merization can be designed to prepare a polymer with the customized properties. These properties can also be adap- ted by preparing the polymer composites. The synthetic polymers most commonly used as enzyme carriers include: poly(vinyl alcohol) (PVA) (Mendes et al.2012) (com- mercial product LentiKats) (Kubac et al.2006); cross- linked poly(vinyl alcohol) (Ozturk and Kilinc2010);
2.2 Organic carriers
Of particular interest
among organic carriers for the
enzyme adsorption is chitosan (Krajewska2004; Nasratun et al.2010; Bayramoglu et al.2012). Chitosan is a polya- minosaccharide obtained from chitin by deacetylation.
poly(N-methylolacrylamide)
(Santos
et
al.
2007);
13

Adsorption (2014) 20:801–821
813
polypropylene (commercial products Accurel EP100 (Torres et al.2008) and Accurel MP1000 (Hita et al.2009); polystyrene in the form of foam (Akdogan and Pazarlioglu2011), in which immobilization is facilitated by a large number of pores; and poly(acrylic acid-co-acrylamide)/ hydrotalcite nanocomposite hydrogels (Zhang et al.2009). An interesting enzyme carrier is the biodegradable and thermo-shrinkable hydroxybutyrate. It is used in the form of poly(hydroxybutyrate) nanoparticles (Deepak et al.2009) and small or large poly(hydroxybutyrate) beads (Mendes et al.2011). Another carrier, poly(o-toluidine) built of particles of o-toluidine isomer has active –NH2groups (Ashly and Mohanan2010). Furthermore, poly(acrylonitrile) (PAN), a polymer widely used in the production of synthetic fibres, as an enzyme carrier is used in the form of electrospun fibres (Sakai et al.2010). PAN mats are about 25lmthick and they are made to have a radius of about 400 nm. The material is very simple and its production is inexpensive. The stiff and elastic PAN car- riers show high porosity and ability to interact with other materials, including enzymes and can be used in the vari- ous types of thereactors.
The carriers for the enzyme adsorption, if prepared in the form of membranes, e.g. as porous hollow fibre mem- branes (Kawakita et al.2002), cotton flannel cloth (Ka- rimpil et al.2012) and nylon membranes (Xu et al.2010), are special as they serve both as an enzyme support and at the same time as a separation phase, which, for instance, canseparatethereagentsofdifferentmolarmasses.
An interesting option seems to be the carriers containing magnetic particles in their structure (Zhang et al.2008;Zhu et al.2009; Tran et al.2012). Such magnetic matrices provide a good control of the process, as upon application of the magnetic field, the immobilized enzyme can be isolated and the catalyzed reaction terminated. Examplesof such magnetic carriers include: a mixture of silicas with iron(II) and iron(III) oxides (Zhu et al.2007);chitosan microspheres (Xie and Wang2012); magnetic poly(acryl- amide-allylglycydyl ether) cryogels (Tuzmen et al.2012); andhydrophobicmagneticparticles(Liuetal.2012a,b).
Commercially available, ion-exchange resins, such as Lewatit (Wu et al.2009), Amberlite IR-120H (Spinelliet al.2012) or Amberlite XAD-2000 and AmberliteXAD-7 (Akdogan and Pazarlioglu2011), typically used in theform of gels, are characterized with a highly developed porous structures and the presence of multiple active groups. These characteristics allow them to act as good enzyme supports.
Beside the materials described above, there are also substances, which although less frequently utilized in enzyme immobilizations, feature good adsorption proper- ties, examples being artificial oil bodies (Hung et al.2008) and olive pomace powder (Yucel2012). An interesting
approach to the immobilization of enzymes is also the use of reverse micelles (Thudi et al.2012), in which the hydrophobic part is directed outside the micelle to allow an enzyme attachment.
2.3 Commercial products
Anexampleofcommerciallyavailableenzymecarriersis StremalineDEAE(ErhardtandJordening2007),whichisa composite made of agarose with a quartz core and dieth- ylaminoethylligandsonthesurface.Anotherexampleare the epoxy-activated polymer supports, such as Eupergit (Katchalski-Katzir and Kraemer2000; Erhardt and Jor- dening2007)commercializedbyRhonHaasandSepabe- ads commercialized by Resindion (Barbosa et al.2013). Both are available in the form of macroporous beads. Eupergit supports are copolymers, of which a maincom- ponent is poly(methacryl amide), while Sepabeads are polystyrenicadsorbents.Commerciallyavailablearealso Celite (Kumar and Kanwar2011) and Celite 545 silica carriers(Bremetal.2011).Theirmaincomponentisdia- tomaceousearth,whichisthesedimentaryrockformedas a result of diatoms exoskeletons deterioration. In thenat- urally occurring form it is admixtured with crystobalite, quartz and alumina. Its particle size varies from a few micrometerstoamillimetre,butinthecommercialproduct it has particles of diameters from 10 to 200 lm. Also worthyofnoteisSepharose,acrosslinked,beaded-formof agarose,apolysaccharidepolymermaterialextractedfrom seaweed. The great advantage of Sepharose is that its surfacecanbechemicallymodifiedinordertobetteradapt it to the functional groups of the protein (Benassi et al.2013). Chitosan is another biopolymer manufactured for theenzymeimmobilizationandmarketedunderthebrandname Chitopearl (Fuji Spinning, Tokyo, Japan) (Krajewska2004). Different Chitopearl beads are produced and they can differ in the type and length of side ligands to be rightly chosen for a particular immobilization. The com- mercialproductsutilizedinenzymeadsorptionalsoinclude a group of polyvinyl supports available under the name Lentikats (Kubac et al.2006), as well as the polymer matrices Accurel EP100 (Torres et al.2008) andAccurel MP1000 (Hita et al.2009).
2.4 Summary of data on enzyme carriers
The foregoing presentation of materials considered and studied for immobilizing enzymes by adsorption, shows that their variety is very rich. It includes organic and inorganic, natural and synthetic materials, that may be configured as beads of different sizes, membranes, fibers, hollow fibers, capsules, sponges in order to best match the conditions of a specific biotransformation in a given
13

814
Adsorption (2014) 20:801–821
bioreactor. Importantly, it also shows that there are no universal carriers for all enzymes and their applications. Effectively, the choice of a specific material is determined by many factors and for each enzyme and each process this should be made individually, as it may happen that a drawback of one material in one process can be its advantageous feature in another one. The followinggeneral comment on the enzyme carrier materials can, however, be proposed. Silicas are perhaps the most common enzyme carriers. Their features, advantageous for this application result chiefly from the well-developed surface area, high availability and low cost. High thermal stability and chemical resistance shown by silica materials are also characteristic for minerals, such as mica or hydroxyapatite. The carriers based on metals, such as titanium, aluminium or zirconium, also show high mechanical strength; how- ever, they show higher affinity to some groups of enzymes, which restricts their application. The magnetic organic and inorganic carriers, which use permits a good control of the enzymatic process, have become very popular but their widespread use is limited by their high cost. For the same reason, the use of carriers based on gold is limited. The interest in materials of natural origin, such as chitin, chitosan or cellulose, stems from their high biocompati- bility and availability, but their application is limited by their selective affinity to certain enzymes, but foremost by their lower durability in the process conditions as com- pared to inorganic materials. By contrast, synthetic poly- mer matrices are widely used for enzyme adsorption, as they can be tailored to suite the specific enzyme and the conditions of a specific process. Moreover, theirproduction is relatively facile and rapid, and what is more, they show high thermal and chemicalresistance.
Lathouder et al.2008; Thudi et al.2012). Glutaraldehyde with the formula CH2(CH2CHO)2contains two reactive aldehyde groups. It is used as a disinfectant and pre- servative. Having high affinity to bacteria, fungi and pro- teins, it is a good enzyme immobilizer. Also, beneficially for the immobilization, its five-atom carbon chain serves as a spacer for enzymes, making their active sites easier accessible for the substrates.
Compounds frequently used as the carrier modifiers for adsorption of enzymes are also silanes, such as 3-amino- propyltrimethoxysilane (Mansur et al.2001; Zhou et al.2011) and 3-aminopropyltriethoxysilane (Falahati et al.2011,2012; Vinoba et al.2012), mercaptopropyl- trimethoxysilane and mercaptopropyltriethoxysilane (Cho et al.2012). The latter two compounds interact stronger with the carrier surface, which is due to the presence of three methoxy or ethoxy groups in their molecules. In the process of surface functionalization, the groups undergo hydrolysis to hydroxyl groups allowing the formation of hydrogen and covalent bonds with the carrier. On the contrary, the presence of –SH or –NH2groups compatible with the enzyme functional groups, facilitates generationof carrier-modifier-enzyme interactions. Other trialkylsilanes used as carrier modifiers include n-octyltriethoxysilane (Zheng et al.2012), phenyltrimethoxysilane, vinyltri- methoxysilane (Hartono et al.2010) and [3-(trimethoxy- silyl)propyl] octadecyl dimethyl ammonium chloride (Tran et al.2012). The attachment of the most common surface modifyingagentstosilicaparticlesisshowninFig.3.
Polymers constitute another group of useful compounds for a carrier modification. Their usefulness originates from the fact that they can be chemically prepared of monomers desired for a given process and their chain lengths can becontrolled. Polyethyleneimine (Karimpil et al.2012), polystyrene (Castro et al.2007) and poly(styrenesulfonate) (Xu et al.2010) are widely applied. In addition tothe branched second generation dendronized polymers (For- nera and Bauer2012), the use of acrylonitrile copolymers was also reported (Godjevargova et al.2006). This com- pound generates interactions with vinyl pyridine, vinyl imidazole andN,N-dimethyl-aminoethyl-methacrylate.
Owing to both acid–base properties and the ability to form hydrogen bonds, amines are also considered as carrier modifiers, the most common among them being diethyl- amine (Kawakita et al.2002), diethylaminoethyl (DEAE) (Karboune et al.2005) and monoaminomethyl-N-amino- ethyl as an agarose gel modifier (Pesic et al.2012)
Also, carboxylic acids have properties classifying them for the use as modifiers. An example of a long-chain car- boxylic acid is erucic acid (Chen et al.2008), while ashort- chain carboxylic acid containing two carboxyl groups and an additional reactive carbonyl group is itaconic acid (Bayramogluetal.2012),bothshowninFig.4.
3 Surface modifying agents
The prerequisite for the successful immobilization of an enzyme by adsorption on a solid carrier is the existence of specific functional groups on the surface of both the enzyme and the carrier. These give rise to the interactions sufficiently strong for the enzyme-carrier binding (adsorption) to occur (Kosaka et al.2007; Gustafsson et al.2012; Wu et al.2012). When such groups are absent, the carrier is subjected to a chemical modification (Cho et al.2012; Mendes et al.2012; Zaidan et al.2012).
The modifying agent should have at least two reactive groups in its molecule; one should enable it to chemically anchor on the carrier and the other one, to physically interact with the enzyme. Typical compounds meeting this condition are bifunctional carbonyl compounds, among them glutaraldehyde being apparently most common (see Fig.4) (Delvaux and Demoustier-Champagne2003; de
13

Adsorption (2014) 20:801–821
815
(a)
O
O
O
O
Si
O
NH
2
H
O
C
HO
OH
H
H
O
HO
O
H
glutaraldehyde
3-aminopropyltriethoxysilane
HO
OH
O
H
O
Si
O
SH
HO
OH
Si
O
O
O
HO
OH
n-octyltriethoxysilane
mercaptopropyltrimethoxysilane
(b)
O
HO
OH
Si
N
OH
OH
H	H
O
HO
OH
O
Si
Si
O
vinyltrimethoxysilane
diethylaminoethyl (DEAE)
O
OH
OH
O
itaconic acid
O
H2N
NH2
HO
OH
OH
OH
H
N
HO
OH
*
n*
polyethyleneimine
(c)
HO
OH
HO
OH
HO
OH

O
OH
SH
HS
Si
Si
O
erucic acid
HO
OH
HO
OH
HO
OH
Fig. 4 Representative surface modifying agents used in enzyme immobilization
(d)
HO
OH
carrier affinity. However, it is possible to propose a carrier that will be optimal for assuring both the desired parame- ters of the process and the target properties of the immo- bilized enzyme.
Enzymes most commonly studied in the immobilized form are lipases (Sakai et al.2010; Adlercreutz2013; Ansorge-Schumacher and Thum2013). Lipasescatalyse the hydrolysis of esters formed by short- and long-chain alcohols, mono- and multi-hydroxides, and saturated and unsaturated carboxylic acids of short and long chains. The catalysts based on lipases are used in the reactions of esterification or transesterification of different substrates (Brem et al.2011; Liu et al.2013; Yu and Fang2013), and in the process of biodiesel production (Salis et al.2010; Mendes et al.2011; Tran et al.2012). A wide use of this group of proteins and their affinity to many carriers permit their immobilization on many organic and inorganic car- riers. Organic carriers seem to be preferred for the immo-bilization of lipases. They include a wide and highly diverse gamut of polymers, such as cross-linked PVA (Ozturk and Kilinc2010) and epoxy activated PVA (Mendes et al.,2012), poly(N-methylol acrylamide) (San- tos et al.2007), small and large poly(hydroxybutyrate) beads (Mendes et al.2011) and polyacrylonitryle electro- spun fibres (Sakai et al.2010), organic matrices of natural origin, including chitosan beads (Nasratun et al.2010), MANAE-agarose and cellulose ultrathin film (Kosaka etal.2007), commercial polymer products, e.g.polypropylene
HO
OH
HO
OH
Si
O
O
Si
HO
OH
OH
HO
HO
OH
Fig. 3
Representative
silica surface modifying
agents
used in
enzyme immobilization, a silica particle grafted with glutaraldehyde, b silica particle modified with 3-aminopropyltriethoxysilane, c silica particle functionalized with mercaptopropyltriethoxysilane, d silica particle grafted with vinyltrimethoxysilane
A new approach to a carrier functionalization is the use of plasma. Oxygen plasma (Gulec2013) and plasma polymerization: allyl alcohol, allyl amine and acrylic acid
were proposed (Labus et al.2012). The high however, a serious disadvantage of the method.
cost
is,
4 Immobilized enzymes
The unquestionable advantage of the enzyme immobiliza- tion by adsorption process is the versatility. The method can be applied for the enzymes of different types, which catalyse diverse sorts of reactions. Clearly, it is notpossible to immobilize any enzyme on any carrier. The range of carriers for a given enzyme is limited by theenzyme-
13

816
Adsorption (2014) 20:801–821
Fig. 5 Lipase immobilization onto glutaraldehyde-modified silica surface
O
H
H
C
HO
OH
NH2
HO
O
H
O
HO
OH
HO
OH
HO
OH
Immobilization
by adsorption
H
O
N
H
C
C
HO
OH
H
HO
O
O
H
OH
HO
HO
OH
HO
OH
membranes Accurel EP100 and
Accurel MP1000 (Hita
nanoparticles modified with a carboxylic surfactant of a long alkyl chain significantly enhanced the activity and enantioselectivity of the immobilized lipases in the organic media (Chen et al.2008). The use of the surfactant in the preparation changed the surface of the nanoparticles from hydrophilic to hydrophobic. It was interpreted that the interaction between the hydrophobic surface of zirconia and lipases induced the conformational rearrangement of lipases into an active, stable form.
Another group of the enzymes of extensive industrial significance, preferably used in the immobilized form, are amylases (Reshmi et al.2006; Bellino et al.2010). The catalysts based on amylases are used on the industrial scale for the hydrolysis of starch. In contrast to lipases, amylases are more specific and their immobilization is possible mostly on inorganic matrices, including mesoporous sili- cas, such as SBA-15 (Ajitha and Suguman2010) or silica thin film (Wang et al.2013), and also silica gel (Nwagu et al.2011), halloysite nanotubes (Zhai et al.2010) and metals, such as zirconium andaluminium.
Laccase is another enzyme used in the industry in the immobilized form (Bayramoglu et al.2012; Xie and Wang2012). Its major task is to oxidize simple phenolic deriv- atives, as well as other compounds containing aromatic moieties. The enzyme can thus be used in bioremediation (Bautista et al.2010). Interestingly, laccase shows an affinity to organic carriers, which is considerably higher comparing to the inorganic carriers. In this context it was immobilized on chitosan membrane (Reshmi et al.2007),
et al.2009), adsorbent Purasorb (Torres et al.2008). Lipases were also immobilized on other materials such as buthyl and octadecyl sepabeads (Branco et al.2010),cotton flannel cloth (Karimpil et al.2012), olive pomace powder (Yucel2012) and commercial ion exchange resin Lewatit. By contrast, among inorganic carriers widely used thereare different silicas, such as mesoporous silicas (Gustafsson et al.2012), e.g. SBA-15 (Yang et al.2013) or MSU-H(Yu and Fang2013), vesicular silica (Wu et al.2012), fumed silica (Kramer et al.2010), silanized silica (Zheng et al.2012), silica sol–gel film (Lee et al.2010) and commercial silica-based products Celite (Brem et al.2011) and Celite 545 (Kumar and Kanwar2011; see Fig.5). Other inorganic carriers used for the adsorption of lipases are zirconia nanoparticles (Chen et al.2008), mica (Zaidan et al.2012), and magnetic carriers (Liu et al.2012a,b; Xie and Wang2012).
An interesting immobilization of lipases was performed in sol–gel derived silica using the multi-walled carbon nanotubes as additives to protect the inactivation of the enzymes during the sol–gel process and to enhance their stability.Theimmobilizedlipasesdisplayednotonlyhigher activities, but also active lifetime as much as five times longer than that of the free enzymes. Similar effects were alsoobservedwhenamesoporoussilicacarrierwasmodified by carboxyl-functionalized ionic liquid (Yang et al.2013).
In contrast, in the process of the lipase adsorption on zirconia nanoparticles, it was demonstrated that the
13

Adsorption (2014) 20:801–821
817
cellulose acetate disc membranes (Labus et al.2012) and commercial cationic resin Amberlite IR-120H (Spinelli et al.2012). Among inorganic carriers, the enzyme was immobilized on different silicas (Tavares et al.2013), e.g. on the commercial mesoporous SBA-15 (Bautista etal.2010), on magnetic mesoporous silica spheres (Zhu et al.2007) and on silica gels functionalized with different organosilanes (Rekuc et al.2010).
Another group of the immobilized enzymes utilized on the industrial scale are oxidases (Kennedy et al.2007; Zhu et al.2009; Fornera and Bauer2012). They are widely applied for catalyzing redox reactions that involve molec- ular oxygen as an electron acceptor. In these reactions oxygen is reduced to water or hydrogen peroxide. Of special significance in this enzyme family is the glucose oxidase. The reason is that this enzyme is applied in glu- cose biosensors, which are exploited as measuring devices in real time, in situ measurements, for instance in food industry, but foremost in medicine. Notably, the immobi- lization of the glucose oxidase was shown to enable con- structing glucose biosensors with improved durabilities, sensitivities, linear ranges and detection limits (Delvaux and Demoustier-Champagne2003; Wu et al.2009; Zhou et al.2011).
Another enzymes from the oxidases family are peroxi- dases, which catalyze the reactions of oxidation,commonly with hydrogen peroxide as a substrate, and are also used in the immobilized form, mainly for the treatment of indus- trial wastewaters (Montiel et al.2007; Pesic et al.2012). The immobilized peroxidases are also used in biosensors for detection of H2O2(Yu and Ju2002). According to the literature, these enzymes are immobilized mainly on inor- ganic silica-based carriers, such as mesoporous silica (Fornera and Bauer2012), commercial SBA-15 (Zhou et al.2011), rod-like and vesicle-like mesoporous silica (Zhou et al.2011), silica gel SG/67 and silica gel100 (Godjevargova et al.2006), and also on magnetic nano- particles based on Fe3O4(Zhu et al.2009), gold nanotubes (Delvaux and Demoustier-Champagne2003) and meso- porous activated carbon matrices MAC 200 and MAC 400 (Kennedy et al.2007). Peroxidases were also immobilized on an inorganic–organic carrier that was made of platinum nanoparticles/graphene sheets/chitosan film (Wu et al.2009), where the enzyme-carrier interactions were medi- ated by the chitosanfilm.
Immobilization by adsorption has also been applied toother enzymes, such as carbonic anhydrases. This group of enzymes catalyzes the reversible interconversion of carbon dioxide and water to bicarbonate and protons. It has been proposed to exploit the reaction in CO2capture and storage (Fransen et al.2013). In the process, commonly known as mineral carbonation (Wanjari et al.2012; Vinoba et al.2012; Zhang et al.2009), carbonic anhydrase serves to
catalyze the CO2hydration. If performed in the presence of Ca2?ions, the reaction is followed by CaCO3precipitation. This bio-based proposal constitutes a new, eco-friendly approach to capture, store or sequester CO2done to avoid the growth of its concentration in the atmosphere. To prepare carbonic anhydrases for this process, the enzymes were adsorbed on inorganic carriers, such as mesoporous silica SBA-15 and mesoporous aluminosilicates, where their stabilities were greatly enhanced, as well as on the complex organic system poly(acrylic acid-co-acrylamide)/ hydrotalcite nanocomposite hydrogel. An interesting example of enzymes of practical applications are also cellulases (Hartono et al.2010; Chang et al.2011), responsible for the hydrolysis of cellulose, for which they were immobilized on mesoporous silicas materials.
Among the noteworthy immobilized enzymes there are also ureases (Krajewska2009b; Marzadori et al.1998;Zhai et al.2010; Krajewska et al.1990). The enzymes are responsible for the hydrolysis of urea to carbonic acid and ammonia (Krajewska2009a, Krajewska et al.2012). The reaction can be exploited in removal of urea from aqueous solutions that is a problem faced in numerous areas, examples being urea-producing industry, agriculture and natural environment, food production and medicine (Kra- jewska2009b). In the latter area, an immobilized urease was considered as a part of the wearable/portable artificial kidney, alternative to the classical hemodialytic device. Important are also analytical applications of immobilized ureases in various biosensing systems, mainly biosensors both for the determinations of urea and of pollutants that are urease inhibitors (Krajewska et al.1997; Krajewskaand Zaborska2007) (spectrometric, potentiometric, conducto- metric, amperometric, acoustic, thermal) (Krajewska2009b). Practical, cost-effective and portable analytical devices, especially useful in the in situ and real-time measurements. The biosensors are predicted to become widely accepted for use, once their storage and operational stabilities areimproved.
An overview of enzymes immobilized by adsorption is presented in Table1along with the carriers, on which they were immobilized, carrier-modifiers, with which carriers had their surfaces modified, techniques that the systems were studied with, and importantly, their properties and possible applications. The overview may thus serve as a guide for making the right choices while preparing enzymes immobilized byadsorption.
5 Conclusions
Enzymes as the effective catalysts have advantageous features, among which the high catalytic efficiency, spec- ificity and mild conditions of operation made them
13

818
Adsorption (2014) 20:801–821
attractive alternatives to the chemical catalysts for a great variety of applications. This has intensified the studies onthe immobilization of the enzymes, in order to improve their catalytic properties. From many methods proposedforthe enzyme immobilization, the most common is the adsorption on the solid carriers. The most important advantage of this immobilization is that a wide gamut of carriers can be used and that the enzymes of practicallyeach class can be immobilized. Equally important is the fact, that this immobilization leaves the enzyme structure intact, which allows enzymes to retain their activity andalso facilitates the transport of the substrates to the enzyme’s active centre. Comparing with the chemicalenzyme immobilizations, a disadvantage of enzyme adsorption is a low stability of the immobilized enzymes, which may lead to a fast washing out of the enzyme from the carrier. However, as follows from the presented surveyof the literature overview, the adsorption remains the fastest and most universal method of the enzymeimmobilization.
Bayramoglu, G., Gursel, I., Yilmaz, M., Arica, M.Y.: Immobilization of laccase on itaconic acid grafted and Cu(II) ion chelated chitosan membrane for bioremediation of hazardous materials.
J. Chem. Technol. Biotechnol. 87, 530–539 (2012)
Bellino, M.G., Regazzoni, A.E., Soler-Illia, G.J.A.A.: Amylase- functionalized mesoporous silica thin films as robust biocatalyst platforms. Appl. Mat. Interfaces 2, 360–365 (2010)
Benassi, V.M., da Silva, T.M., Pesslea, B.C., Guisan, J.M., Mateo,C., Lima, M.S., Jorge, J.A., de Polizeli, M.L.T.M.: Immobilization and biochemical properties of b-xylosidase activated by glucose/ xylose fromAspergillus nigerUSP-67 withtransxylosylation activity.J.Mol.Catal.B89,93–101(2013)
Bhattacharyya, M.S., Singh, A., Banerjee, U.C.: Immobilization of intracellular carbonyl reductase fromGeotrichym candidumfor the stereoselective reduction of 1-naphthyl ketone. Bioresour. Technol. 101, 1581–1586 (2010)
Brady, D., Jordon, J.: Advances in enzyme immobilisation. Biotech- nol. Lett. 31, 1639–1650 (2009)
Branco, R.V., Gutarra, M.L.E., Freire, D.M.G., Almeida, R.V.: Immobilization and characterization of a recombinant thermo- stable lipase (Pf2001) fromPyrococcus furiosuson suports with different degrees of hydrophobicity. Enzyme Res. 2010, 1–8 (2010)
Brem, J., Turcu, M.C., Paizs, C., Lundell, K., Tosa, M.I., Irimie,F.D., Kanerva, L.T.: Immobilization to improve the propeties ofPseudomonas flourescenslipase for the kinetic resolution of 3-aryl-3-hydroxyesters.Proc.Biochem.47,119–126(2011)
Bronshyteyn, M., Steinberg, D.: Immobilization of fructosyltransfer- ase fromStreptococcus mutanson hydroxyapatite surfacesinduces the formation of multimeric complexes. Lett. Appl. Microbiol. 34, 205–209 (2002)
Cao, L., van Langen, L., Sheldon, R.A.: Immobilised enzymes:carrier-bound or carrier-free? Curr. Opin. Biotechnol. 14, 387–394 (2003)
Cao, L.: Immobilised enzymes: science or art? Curr. Opin. Biotech- nol. 9, 217–226 (2005)
Carrea, G., Riva, S.: Properties and synthetic applications of enzymesin organic solvents. Angew. Chem. Int. Ed. 39, 2226–2254(2000)
Castro, L.B.R., Silva, F.F., Carmona-Ribeiro, A.M., Kappl, M., Petri,D.F.S.: Immobilization of hexokinase onto chitozan decorated particles. J. Phys. Chem. B 111, 8520–8526 (2007)
Chang, R.H.Y., Jang, J., Wu, K.C.W.: Cellulaseimmobilizedmesoporous silica nanocatalysts for efficientcellulose-to-glucose conversion. Green Chem. 13, 2844–2850(2011)
Chen, Y.Z., Yang, C.T., Ching, C.B., Xu, R.: Immobilization oflipases on hydrophobilized zirconia nanoparticles: highly enan-tioselective and reusable biocatalysts. Langmuir 24, 8877–8884 (2008)
Cho, E.J., Jung, S., Kim, H.J., Lee, Y.G., Nam, K.C., Lee, H.J., Bae,
H.J.: Co-immobilization of three cellulases on Au-doped mag-netic silica nanoparticles for the degradation of cellulose. Chem. Commun. 48, 886–888 (2012)
Choma, J., Kloske, M., Jaroniec, M., Klinik, J.: Benzene adsorptionisotherms on MCM-41 and their use for pore size analysis. Adsorption 10, 195–203 (2004)
Cowan, D.A., Fernandez-Lafuente, R.: Enhancing the functional properties of thermophilic enzymes by chemical modificationand immobilization. Enzyme Microb. Technol. 49, 326–346(2011)
de Lathouder, K.M., van Benthem, D.T.J., Wallin, S.A., Mateo, C., Fernandez Lafuente, R., Guisan, J.M., Kapteijn, F., Moulijn, J.A.: Poliethyleneimine (PEI) functionalized ceramic monoliths as enzyme carriers: preparation and performance. J. Mol. Catal. B 50, 20–27 (2008)
Acknowledgments This work was supported by research Grant no. 3/32/443–DS-PB/2014 from Poznan University of Technology,Poznan´,Poland(TJ,JZ),andbyDSWCh/43fromtheFacultyofChemistryoftheJagiellonianUniversity,Krako´w,Poland(BK).
Open Access This article is distributed under the terms of the Creative Commons Attribution License which permits any use, dis- tribution, and reproduction in any medium, provided the original author(s) and the sourceare credited.
References
Adlercreutz, P.: Immobilisation and application of lipases in organic media. Chem. Soc. Rev. 42, 6406–6436 (2013)
Ajitha, S., Suguman, S.: Tuning mesoporous molecular sieve SBA-15 for the immobilization of a-amylase. J. Porous Mater. 17, 341–349 (2010)
Akdogan, H.A., Pazarlioglu, N.K.: Fluorene biodegradation byP.osteratus-part II: biodegradation by immobilized cells in arecycled packed bed reactor. Proc. Biochem. 46, 840–846 (2011)Alatorre-Meda, M., Taboada, P., Sabin, J., Krajewska, B., Varela,
L.M., Rodriguez, J.R.: DNA-chitosan complexation: a dynamic light scattering study. Colloid Surf. A 339, 145–152 (2009)
Ansorge-Schumacher, M.B., Thum, O.: Immobilised lipases in the cosmetics industry. Chem. Soc. Rev. 42, 6475–6490 (2013)
Ashly, P.C., Mohanan, P.V.: Preparation and characterization ofRhizopusamyloglucosidase immobilized on poly(o-toluidine). Process Biochem. 45, 1422–1426 (2010)
Barbosa, O., Torres, R., Ortic, C., Berenguer-Murcia, A., Rodrigues, R.C., Fernandez-Lafuente, R.: Heterofunctional supports in enzyme immobilization: from traditional immobilization proto- cols to opportunities in tuning enzyme properties. Biomacro- molecules 14, 2433–2462 (2013)
Bautista, L.F., Morales, G., Sanz, R.: Immobilization strategies for laccaseTrametes versicoloron mesostructured silica materials and the application to the degradation of naphthalene. Bioresour. Technol. 101, 8541–8548 (2010)
13

Adsorption (2014) 20:801–821
819
Deepak, V., Pandian, S.B.R.K., Kalishwaralal, K., Gurunathan, S.: Purification, immobilization and characterization of nattokinaseon PHB nanoparticles. Bioresour. Technol. 100, 6644–6646 (2009)
Delvaux, M., Demoustier-Champagne, S.: Immobilisationofglucoseoxidasewithinmetallicnanotubesarraysforapplicationtoenzyme bionsensors. Biosens. Bioelectron. 18,943–951(2003)DiCosimo, R., McAuliffe, J., Poulose, A.J., Bohlmann,G.:Industrialuseofimmobilizedenzymes.Chem.Soc.Rev.42,6437–6474
(2013)
Erhardt, F.A., Jordening, H.J.: Immobilization of dextranasefromChaetomium erraticum. J. Biotechnol. 131, 440–447 (2007) Falahati,M.,Ma’mani,L.,Sabuory,A.A.,Shafiee,A.,Foroumadi,A.,
Badiei, A.R.: Aminopropyl functionalized cubic Ia3d mesopor- ous silica nanoparticle as an efficient suport for immobilizationof superoxide dismutase. Biochim. Biophys. Acta. 1814, 1195–1202 (2011)
Falahti, M., Saboury, A.A., Ma’mani, L., Shafiee, A., Rafieepour, H.A.: The effect of functionalization of mesoporous silicananoparticlesontheinteractionandstabilityofconfinedenzyme.Int.J.Biol.Macromol.50,1048–1054(2012)
Fargues, C., Bailly, M., Grevillot, G.: Adsorption of BSA andhemoglobin on hydroxyapatite support: equilibria and multi- component dynamic. Adsorption 4, 5–16 (1998)
Fernandez-Lafuente, R.: Stabilization of multimeric enzymes: strat-egies to prevent subunit dissociation. Enzyme Microb. Technol.45, 405–418 (2009)
Fornera, S., Bauer, T., Dieter Schluter, A., Walde, P.: Simple enzymeimmobilization inside glass tubes for enzymatic cascade reac- tions. J. Mater. Chem. 22, 502–511 (2012)
Fransen, M.C.R., Steunenberg, P., Scott, E.L., Zuilhof, H., Sanders,J.P.M.: Immobilised enzymes in biorenewables production. Chem. Soc. Rev. 42, 6491–6533 (2013)
Garcia-Galan, C., Berenguer-Murcia, A., Fernandez-Lafuente, R.,Rodrigues, R.C.: Potential of different enzyme immobilizationstrategies to improve enzyme performance. Adv. Synth. Catal. 353, 2885–2904 (2011)
Geng, L., Li, N., Xiang, M., Wen, X., Xu, D., Zhao, F., Li, K.: Thecovalent immobilization of trypsin at the galleries of layered c- zirconium phosphate. Colloid Surf. B 30, 99–109 (2003)
Godjevargova, T., Nenkova, R., Konsulov, V.: Immobilization ofglucose oxidase by acronitrile copolymer coated silica supports. J. Mol. Catal. B 38, 59–64 (2006)
Grabicka, B.E., Jaroniec, M.: Adsorption properties of ordered mesoporous silicas synthesized in the presence of block copoly-mer Pluronic F127 under microwave irradiation. Adsorption 16, 385–396 (2010)
Gray, C.J., Weissenborn, M.J., Eyers, C.E., Plitsch, S.L.: Enzymaticreactions on immobilised substrates. Chem. Soc. Rev. 42, 6378–6405 (2013)
Grudzien´,R.M.,Grabicka,B.E.,Felix,R.,Jaroniec,M.:Polymer-
templated organosilicas with hexagonally ordered mesopores:the effect of organosilane addition at different synthesis stages. Adsorption 13, 323–329(2007)
Grudzien´,R.M.,Grabicka,B.E.,Jaroniec,M.:Adsorptionand
structural properties of channel-like and cage-like organosilicas. Adsorption 12, 293–308 (2006)
Gulec, H.A.: Immobilization of b-galactosidase fromKluyveromyceslactisonto polymeric membrane surfaces: effect of surface characteristics. Colloid Surf. B 104, 83–90 (2013)
Gupta, A., Prabhu, K.A.: Immobilization and properties of dextran-sucrase fromLeuconostoc mesenteroidesculture, LM1. J. Gen. Appl. Microbiol. 41, 399–407 (1995)
Gustafsson, H., Johansson, E.M., Barrabino, A., Oden, M.,Holmberg, K.:ImmobilizationoflipasefromMucormieheiandRhizopus
oryzaeonto mesoporus silca-the effect of varied particle size and morphology. Colloid Surf. B 100, 22–30 (2012)
Hanefeld, U., Cao, L., Magner, E.: Enzyme immobilisation: funda-mentals and application. Chem. Soc. Rev. 42, 6211–6212 (2013)
Hanefeld, U., Gardosi, L., Magner, E.: Understanding enzyme immobilisation. Chem. Soc. Rev. 38, 453–468 (2009)
Hartmann, M., Kostrov, X.: Immobilization of enzymes on porous silicas-benefits and challenges. Chem. Soc. Rev. 42, 6277–6289 (2013)
Hartono, S.B., Qiao, S.Z., Liu, J., Jack, K., Ladewig, B.P., Hao, Z., Lu, G.Q.M.: Functionalized mesoporous silica with very large pores for cellulase immobilization. J. Phys. Chem. 83, 8353–8362 (2010)
Hernandez, K., Fernandez-Lafuente, R.: Control of protein immobi- lization: coupling immobilization and site-directed mutagenesis to improve biocatalyst or biosensor performance. Enzyme Microb. Technol. 48, 107–122 (2011)
Hita, E., Robles, A., Camacho, B., Gonzalez, P.A., Esteban, L., Jimenez, M.J., Munio, M.M., Molina, E.: Production of struc- tured triacylglycerols by acidolysis catalyzed by lipases immo- bilized in a packed bed reactor. Biochem. Eng. J. 46, 257–264 (2009)
Honarkar, H., Barikani, M.: Applications of biopolymers. I. Chitosan.
Monatsh Chem. 140, 1403–1420 (2009)
Hung, Y.J., Peng, C.C., Tzen, J.T.C., Chen, M.J., Liu, J.R.:
Immobilization ofNeocallimastix patriciarumxylanase on artificial oil bodies and statistical optimization of enzyme activity. Bioresour. Technol. 99, 8662–8666 (2008)
Hwang, E.T., Gu, M.B.: Enzyme stabilization by nano/microsized hybrid materials. Eng. Life Sci. 1, 49–61 (2013)
Iyer, P.V., Ananthanarayan, L.: Enzyme stability and stabilization- aqueous and non-aqueous environment. Process Biochem. 43, 1019–1032 (2008)
Jaroniec, M., Fulvio, P.F.: Standard nitrogen adsorption data for a- alumina and their use for characterization of mesoporous alumina-based materials. Adsorption 19, 475–481 (2013)
Karboune, S., Neufeld, R., Kermasha, S.: Immobilization and biocatalysis of chlorophyllase in selected organic solvent systems. J. Biotech. 120, 273–283 (2005)
Karimpil, J.J., Melo, J.S., D’Souza, S.F.: Immobilization of lipase on cotton cloth using the layer-by-layer self-assemble technique. Int.J.Biol.Macromol.50,300–302(2012)
Katchalski-Katzir,E.,Kraemer,D.M.:Eupergit®C,acarrierforimmobilization of enzymes of industrial potential. J. Mol. Catal. B 10, 157–176 (2000)
Kawaguti, H.Y., Hoffmann Carvalho, P., Figueira, J.A., Sato, H.H.: Immobilization ofErwiniasp. 12 cells in alginate-gelatin matrix and conversion of sucrose into osomaltulose using response surface methodology. Enzyme Res. 1, 1–8 (2011)
Kawakita, H., Sugita, K., Saito, K., Tamada, M., Sugo, T., Kawam- oto, H.: Production of cycloisomaltooligosacharides from dex- tran using enzyme immobilized in multilayers porous membranes. Biotechnol. Prog. 18, 465–469 (2002)
Kennedy, L.J., Selvi, P.K., Padmanabhan, A., Hema, K.N., Sekaran, G.: Immobilization of polyphenol oxidase onto mesoporous activated carbons-isotherm and kinetic studies. Chemosphere 69, 262–270 (2007)
Klibanov, A.M.: Improving enzymes by using them in organic solvents. Nature 409, 241–246 (2001)
Kosaka, P.M., Kawano, Y., El Seound, O.A., Petri, D.F.S.: Catalytic activity of lipase immobilized onto ultrathin films of cellulose esters. Langmuir 23, 12167–12173 (2007)
Krajewska, B., Leszko, M., Zaborska, W.: Urease immobilized on chitosan membrane. Preparation and properties. J. Chem. Tech. Biotechnol. 48, 337–350 (1990)
13

820
Adsorption (2014) 20:801–821
Krajewska, B., Zaborska, W., Leszko, M.: Inhibition of chitosan-immobilized urease by boric acid as determined by integration methods. J. Mol. Catal. B 3, 231–238 (1997)
Krajewska, B.: Application of chitin- and chitosan-based materialsforenzyme immobilizations: a review. Enzyme Microb. Technol. 35, 126–139(2004)
Krajewska, B.: Membrane-based processes performed with use ofchitin/chitosan materials. Sep. Purif. Tech. 41, 305–312 (2005)Krajewska, B., Zaborska, W.: Double mode of inhibition-inducinginteractions of 1,4-naphthoquinone with urease. Arylation vsoxidation of enzyme thiols. Bioorg. Med. Chem. 15, 4144–4151
(2007)
Krajewska,B.,Wydro,P.,Jan´czyk,A.:Probingthemodesofantibacterial activity of chitosan. Effects of pH and molecularweight on chitosan interactions with membrane lipids inLangmuir films. Biomacromolecules 12, 4144–4152(2011)
Krajewska, B., Wydro, P., Kyzioł, A.: Chitosan as a subphase disturbant of membrane lipid monolayers. The effect of temper-ature at varying pH: I. DPPG. Colloid Surf. A 434, 349–358(2013a)
Krajewska, B., Kyzioł, A., Wydro, P.: Chitosan as a subphase disturbant of membrane lipid monolayers. The effect of temper-ature at varying pH: II. DPPC and cholesterol. Colloid Surf. A 434, 359–364 (2013b)
Krajewska, B.: Ureases I. Functional, catalytic and kinetic properties: a review. J. Mol. Cat. B 56, 9–21 (2009a)
Krajewska, B.: Ureases. II. Properties and their customizing byenzyme immobilizations: a review. J. Mol. Cat. B 59, 22–40 (2009b)
Krajewska, B., van Eldik, R., Brindell, M.: Temperature- and pressure-dependent stopped-flow kinetic studies of jack-beanurease. Implications for the catalytic mechanism. J. Biol. Inorg. Chem. 17, 1123–1134 (2012)
Kramer, M., Cruz, J.C., Pfromm, P.H., Rezac, E., Czermak, P.:Enantioselective transestrification byCandida antarcticalipase B immobilized on fumed silica. J. Biotechnol. 150, 80–86(2010)
Kubac, D., Cejkova, A., Masak, J., Jirku, V., Lemaire, M., Gallienne,E., Bolte, J., Stloukal, R., Martinkova, L.: Biotransformation ofnitriles byRhodococcus equiA4 immobilized in LentiKats. J.Mol.Catal.B39,59–61(2006)
Kumar, A., Kanwar, S.S.: Synthesis of ethyl ferulate in organicmedium using celite-immobilized lipase. Bioresour. Technol. 102, 2162–2167 (2011)
Kwon, S.W., Jeong, B.O., Lee, E.H., Kim, Y.S., Jung, Y.:Conductingpolimer silica composites for immoilization of enzymes. Bull.Korean Chem. Soc. 33, 1593–1596(2012)
Labus, K., Gancarz, I., Bryjak, J.: Immobilization of laccase andtyrosinase on untreated and plasma-terated cellulosic andpolyamide membranes. Mater. Sci. Eng. C 32, 228–235 (2012)
Lee, S.H., Doan, T.T.N., Won, K., Ha, S.H., Koo, Y.M.: Immobi-
lization of lipase within carbon nanotube-silica composites fornon-aqueous reaction systems. J. Mol. Catal. B 62, 169–172 (2010)
Liese, A., Hilterhaus, L.: Evaluation of immobilized enzymes forindustrial applications. Chem. Soc. Rev. 42, 6236–6249 (2013)
Liu, C.H., Huang, C.C., Wang, Y.W., Lee, D.J., Chang, J.S.: Biodiesel production by enzymatic transestrification catalyzedBrukholderialipase immobilized in hydrophobic magneticparticles. Appl. Energy 100, 41–46 (2012a)
Liu, N., Wang, Y., Zhao, Q., Cui, C., Fu, M., Zhao, M.: Immobi-lisation of lecitase ultra for producion of diacylglycerols by glycerolysis of soybean oil. Food Chem. 134, 301–307 (2012b)
Liu, Q., Kong, X., Zhang, C., Chen, Y., Hua, Y.: Immobilisation of a hydroperoxide lyase and comparative enzymological studies oftheimmobilisedenzymewithmembrane˛-boundenzyme.J.Sci.Food Agric. 93, 1953–1959 (2013)
Magner, E.: Immobilisation of enzymes on mesoporous silicate materials. Chem. Soc. Rev. 42, 6213–6222 (2013)
Mansur, H.S., Orefice, R.L., Lobato, Z.P., Vasconcelos, W.L., Mansur, E.S., Machado, L.J.C.: Adsorption/desorption behavior of bovine serum albumin and porcine insulin on chemically patterned porous gel networks. Adsorption 7, 105–116 (2001)
Marzadori, C., Miletti, S., Gessa, C., Ciurli, S.: Immobilization of jack bean urease on hydroxyapatite: urease immobilization on alkalinesoils.SoilBiol.Biochem.30,1485–1490(1998)
Mateo, C., Palomo, J.M., Fernandez-Lafuente, G., Guisan, J.M., Fernandez-Lafuente, R.: Improvement of enzyme activity, stability and selectivity via immobilization techniques. Enzyme Microb. Technol. 40, 1451–1463 (2007)
Mendes, A.A., Freitas, L., de Carvalho, A.K.F., de Oliviera, P.C., de Castro, H.F.: Immobilization of a commercial lipase fromPenicillium camembertii(Lipase G) by different strategies. Enzyme Res. 2011, 1–8 (2011)
Mendes, A.A., Oliveira, P.C., Velez, A.M., Giordano, R.C., de Giordano, R.L.C., de Castro, H.F.: Valuation of immobilized lipases on poly-hydroxybutyrate beads to catalyze biodiesel synthesis. Int. J. Biol. Macromol. 50, 503–511 (2012)
Montiel, C., Terres, E., Dominguez, J.M., Aburto, J.: Immobilization of chloroperoxidase on silica-based materials for 4,6-dimethyl dibenzophene oxidation. J. Mol. Catal. B 48, 90–98 (2007)
Nara, T.Y., Togashi, H., Sekikawa, C., Inoh, K., Hisamatsu, K., Sakaguchi, K., Mizukami, F., Tsunoda, T.: Functional immobi- lizationof racemase by adsorption on folded-sheet mesoporous silica. J. Mol. Catal. B 64, 107–112 (2010)
Nasratun, M., Hasrul, A.S., Sureena, A., Nurul Aini, M.A., Ruwaida, A.R., Shalyda, M.S., Ideris, A., Rozaimi, A.S., Sharifuddin,J.H., Ahamad Nordin, N.I.A.: Immobilization of lipase fromCandidarugosaon chitosan beads for transesterification reaction. J.Appl. Sci. 10, 2701–2709(2010)
Nwagu, T.N., Okolo, B.N., Aoyagi, H.: Immobilization of raw starch digesting amylase on silica gel: a comparative study. Afr. J. Biotechnol. 10, 15989–15997(2011)
Ozturk, T.K., Kilinc, A.: Immobilization of lipase in organic solvent in the presence of fatty acid additives. J. Mol. Catal. B 67, 214–218 (2010)
Pesic, M., Lopez, C., Alvaro, G., Lopez-Santin, J.: A novel immobilized chloroperoxidase biocatalyst with improved stabil- ity for the oxidation of amino alcohols to amino aldehydes. J.Mol.Catal.B84,144–151(2012)
Rekuc´,A.,Bryjak,J.,Szyman´ska,K.,Jarze˛bski,A.B.:Verystablesilica-gel-bound laccase biocatalysts for the selective oxidation in continuous systems. Bioresour. Technol. 101, 2076–2083 (2010)
Reshmi, R., Sanjay, G., Sugunan, S.: Enhanced activity and stability of a-amylase immobilized on alumina. Catal. Commun. 7, 460–465 (2006)
Reshmi, R., Sanjay, G., Sugunan, S.: Immobilization of a-amylase on zirconia: a heterogeneous biocatalyst for starch hydrolysis.Catal. Commun. 8, 393–399(2007)
Rodrigues, R.C., Ortiz, C., Berenguer-Murcia, A.,Torres,R.,Fernandez-Lafuente, R.: Modifying enzyme activityandselec-tivity by immobilization. Chem. Soc. Rev. 42,6290–6307(2013)Rodrigues, R.C., Berenguer-Murcia, A., Fernandez-Lafuente,R.:
Coupling chemical modification and immobilization to improve the catalytic performance of enzymes. Adv. Synth. Catal. 353, 2216–2238 (2011)
Sakai, S., Liu, Y., Yamaguchi, T., Watanabe, R., Kawabe, M., Kawakami, K.: Production of butyl-biodiesel using lipase physically-adsorbed onto electrospun polyacrylonitryle fibers. Bioresour. Technol. 101, 7344–7349 (2010)
Salis, A., Casula, M.F., Bhattacharyya, M.S., Pinna, M., Solinas, V., Monduzzi, M.: Physical and chemical lipase adsorption on SBA-
13

Adsorption (2014) 20:801–821
821
15: effect of different interactions on enzyme loading andcatalytic performance. Chem. Cat. Chem. 2, 322–329 (2010)
Santos, J.C., Nunes, G.F.M., Moreira, A.B.R., Perez, V.H., de Castro, H.F.: Characterization ofCandida rugosalipase immobilized onpoly(N-methyloacrylamide) and its application in butyl butyrate synthesis. Chem. Eng. Technol. 30, 1255–1261 (2007)
Sheldon, R.A., van Pelt, S.: Enzyme immobilisation in biocatalysis:why, what and how? Chem. Soc. Rev. 42, 6223–6225 (2013)
Sheldon, R.A.: Enzyme immobilization: the quest for optimum performance. Adv. Synth. Catal. 49, 1289–1307 (2007)
Spinelli, D., Fatarella, E., Di Michele, A., Pogni, R.: Immobilizationof fungal (Trametes versicolor) laccase onto Amberlite IR-120Hbeads: optimization and characterization. Proc. Biochem. 48, 218–223(2012)
Tavares, A.P.M., Rodriguea, O., Fernandez-Fernandez, M., Domin- guez, A., Moldes, D., Sanroman, M.A., Macado, E.A.: Immo- bilization of laccase on modified silica: stabilization, thermal inactivation and kinetic bahaviour in 1-ethyl-3-methylimidazo-lium ethylsulfate inonic liquid. Bioresour. Technol. 131, 405–412 (2013)
Thorn, C., Gustafsson, H., Olsson, L.: Immobilization of feruloylesterases in mesoporous materials leads to improved transestri- fication yield. J. Mol. Catal. B 72, 57–64 (2011)
Thudi, L., Jasti, L.S., Swarnalahta, Y., Fadnavis, N.W., Mulani, K., Deokar, S., Ponratham, S.: Enzyme immobilization on epoxysupports in reverse micellar media: prevention of enzyme denaturation. J. Mol. Catal. B 74, 54–62 (2012)
Torres, P., Reyes-Duarte, D., Lopez-Cortes, N., Ferrer, M., Ballest-eros, A., Plou, F.J.: Acetylation of vitamin E byCandidaantarcticalipase B immobilized on diffrent carriers. Proc. Biochem. 43, 145–153 (2008)
Tran, D.T., Chen, C.L., Chang, J.S.: Immobilization ofBrukholderiasp. lipase on a ferric nanocomposite for biodiesel production. J. Biotech. 158, 112–119(2012)
Tuzmen, N., Kalburcu, T., Denizli, A.: Immobilization of catalase viaadsorption onto metal-chelated affinity cryogels. Proc. Biochem.47, 26–33 (2012)
Vinoba, M., Bhagiyalakshmi, M., Jeong, S.K., Yoon, Y.I., Nam,S.C.: Immobilization of carbonic anhydrase on spherical SBA-15 forhydration and sequestration of CO2. Colloid Surf. B 90, 91–96 (2012)
Wang, S., Su, P., Ding, F., Yang, Y.: Immobilization of cellulase onpolyamidoamine dendrimer-grafted silica. J. Mol. Catal. B 89, 35–40 (2013)
Wanjari, S., Pabhu, C., Satyanarayana, T., Vinu, A., Rayalu, S.: Immobilization of carbonic anhydrase on mesoporous alumino-silicate for carbonation reaction. Micropor. Mesopor. Mater. 160, 151–158(2012)
Weber, E., Sirim, D., Schreiber, T., Thomas, B., Pleiss, J., Hunger, M., Glaser, R., Urlacher, V.B.: Immobilization of P450 BM-3monooxygenase on mesoporous molecular sives with different pore diameters. J. Mol. Catal. B 64, 29–37 (2010)
Wu, C., Zhou, G., Jiang, X., Ma, J., Zhang, H., Song, H.: Activebiocatalysts based onCandida rugosalipase immobilized in versicular silica. Proc. Biochem. 47, 953–959 (2012)
Wu, H., Wang, J., Kang, X., Wang, C., Wang, D., Liu, J., Aksay,I.A., Lin, Y.: Glucose biosensor based on immobilization of glucose oxidase in pltinum nanoparticles/graphene/chitosan nanocom- posite film. Talanta 80, 403–406(2009)
Xiao, P., Lv, X., Deng, Y.: Immobilization of chymotrypsin on silica beads based on high affinity and specificity aptamer and its applications. Anal. Lett. 45, 1264–1273 (2012)
Xie, W., Wang, J.: Immobilized lipase on magnetic chitosan microspheres for transestrification of soybean oil. Biomass Bioenergy 36, 373–380 (2012)
Xu, F., Wang, W.H., Tan, Y.J., Bruening, M.L.: Facile trypsin immobilization in polymeric membranes for rapid, efficient, protein digestion. Anal. Chem. 82, 10045–10051 (2010)
Yang, J., Hu, Y., Jiang, L., Zou, B., Jia, R., Huang, H.: Enhancing the catalytic properties of porcine pancreatic lipase by immobiliza- tion on SBA-15 modified by functionalized ionic liquid. Biochem. Eng. J. 70, 46–54 (2013)
Yu, J., Ju, H.: Preparation of porous titania sol–gel matrix for immobilization of horseradish peroxidase by a vapor deposition method. Anal. Chem. 74, 3579–3583 (2002)
Yu, W., Fang, M., Tong, D.S., Shao, P., Xu, T., Zhou, C.: Immobilization ofCandida rugosalipase on hexagonal meso- porous silca and selective estrification in nonaqueous medium. Biochem. Eng. J. 70, 97–105 (2013)
Yucel, Y.: Optimization of immobilization conditions ofThermomy-ces lanuginosuslipase on olive pomace powder using response methodology. Biocatal. Agric. Biotechnol. 1, 39–44 (2012)
Zaidan, U.H., Rahman, M.B.A., Othman, S.S., Basr, M.,Abdulmalek, E., Rahman, R.N.Z.R.A., Salleh, A.B.: Biocatalytic production of lactose ester catalysed by mica-based immobilised lipase. Food Chem. 131, 199–205(2012)
Zhai, R., Zhang, B., Liu, L., Xie, Y., Zhang, H., Liu, J.: Immobi- lization of enzyme biocatalyst on natural halloysite nanotubes. Catal. Commun. 12, 259–263 (2010)
Zhang, B., Xing, J.M., Liu, H.Z.: Synthesis and characterization of superparamagnetic poly(urea-formaldehyde) adsorbents and their use for adsorption of flavonoids fromGlycyrrhiza uralensisFisch. Adsorption 14, 65–72(2008)
Zhang, Y.T., Zhi, T.T., Zhang, L., Huang, H., Chen, H.L.: Immo- biliation of carbonic anhydrase by embedding and covalent coupling into nanocomposite hydrogel containig hydrotalcite. Polymer 50, 5693–5700 (2009)
Zhao, H.: Methods for stabilizing and activating enzymes in ionic liquids: a review. J. Chem. Technol. Biotechnol. 85, 891–907 (2010)
Zheng, M.M., Lu, Y., Dong, L., Guo, P.M., Deng, Q.C., Li, W.L.,
Feng, Y.Q., Huang, F.H.: Immobilization ofCandida rugosalipase on hydrophobic/strong cation-exchange functional silica particles for biocatalytic synthesis of phytosterol esters. Biore- sour. Technol. 115, 141–146 (2012)
Zhou, G., Fung, K.K., Wong, L.W., Chen, Y., Renneberg, R., Yang, S.: Immobilization of glucose oxidase on rod-like and vesicle- like mesoporous silica for enhancing current responses of glucose biosensors. Talanta 84, 659–665 (2011)
Zhu, H., Pan, J., Hu, B., Yu, H.L., Xu, J.H.: Immobilization of glycolate oxidase fromMedicago falcataon magnetic nanopar- ticles for applications in biosynthesis of glyoxylic acid. J. Mol. Catal. B 61, 174–179 (2009)
Zhu, Y., Kaskel, S., Shi, J., Wage, T., Van Pee, K.H.: Immobilization ofTramtes versicolorlaccase on magnetically separable meso- porous silica spheres. Chem. Mater. 19, 6408–6413 (2007)
13