Nalepa et al. Cancer Nano (2020) 11:2
https://doi.org/10.1186/s12645-020-00058-4
# Cancer Nanotechnology
Correspondence:
maciej.serda@us.edu.pl
1 Institute of Chemistry,
University of Silesia
in Katowice, Katowice, Poland
Full list of author information
is available at the end of the
article
Abstract
Background: The first-line chemotherapy drug that is used to treat pancreatic ductal
adenocarcinoma is gemcitabine. Unfortunately, its effectiveness is hampered by its
chemo-resistance, low vascularization and drug biodistribution limitations in the tumor
microenvironment. Novel nanotherapeutics must be developed in order to improve
the prognosis for patients with pancreatic cancer.
Results: We developed a synthetic methodology for obtaining a water-soluble nano-
conjugate of a [60]fullerene-glycine derivative with the FDA-approved drug gemcit-
abine (nanoC60 GEM) . The proposed synthetic protocol enables a highly water-soluble
[60]fullerene-glycine derivative (6) to be obtained, which was next successfully conju-
gated with gemcitabine using the EDCI/NHS carbodiimide protocol. The desired nano-
conjugate was characterized using mass spectrometry and DLS, IR and XPS techniques.
The photogeneration of singlet oxygen and the superoxide anion radical were studied
by measuring 102 near-infrared luminescence at 1270 nm, followed by spin trapping
of the DMPO adducts by EPR spectroscopy. The biological assays that were performed
indicate that there is an inhibition of the cell cycle in the S phase and the induction of
apoptosis by nanoC60GEM.
Conclusion: In this paper, we present a robust approach for synthesizing a highly
water-soluble [60]fullerene nanoconjugate with gemcitabine. The performed biological
assays on pancreatic cancer cell lines demonstrated cytotoxic effects of nanoC60GEM,
which were enhanced by the generation of reactive oxygen species after blue LED
irradiation of synthesized fullerene nanomaterial.
Keywords: [60]Fullerene, Nanoconjugate, Gemcitabine, Pancreatic cancer
Background
The rapid development of nanotechnology is of great interest to researchers focused
on translational medicine and novel targeted cancer treatment (Kim et al. 2010).
The most popular applications of nanotherapeutics include diagnosis and treatment
© The Author(s) 2020. This article is licensed under a Creative Commons Attribution 4.0 International License, which permits use, sharing,
adaptation, distribution and reproduction in any medium or format, as long as you give appropriate credit to the original author(s) and the
source, provide a link to the Creative Commons licence, and indicate if changes were made. The images or other third party material in this
article are included in the article's Creative Commons licence, unless indicated otherwise in a credit line to the material. If material is not
included in the article's Creative Commons licence and your intended use is not permitted by statutory regulation or exceeds the permitted
use, you will need to obtain permission directly from the copyright holder. To view a copy of this licence, visit http://creativecommons.org/
licenses/by/4.0/. The Creative Commons Public Domain Dedication waiver (http://creativecommons.org/publicdomain/zero/] .0/) applies
to the data made available in this article, unless otherwise stated in a credit line to the data.
A [60]fullerene nanoconjugate
with gemcitabine: synthesis, biophysical
properties and biological evaluation for treating
pancreatic cancer
## Paweł Nalepa1, Robert Gawecki2, Grzegorz Szewczyk3, Katarzyna Balin2, Mateusz Dulski4, Mieczysław Sajewicz1, Anna Mrozek-Wilczkiewicz2, Robert Musioł1, Jaroslaw Polanski1 G and Maciej Serda1*©
# ReseArch
# Open Access

Nalepa et al. Cancer Nano
(2020) 11:2
Page 2 of 21
of cancer, targeted drug delivery systems and in vivo imaging (Chow and Ho 2013;
Dawidczyk et al. 2014). The nanotechnology approach has been used by medicinal
chemists to design potential drugs that can easily break through almost any biological
barrier. Engineered nanoparticles, including carbon nanomaterials, can enter tumors
via their leaky vessels and remain there due to the weak drainage in the tumor micro-
environment. This phenomenon is called the enhanced permeability and retention
effect (EPR effect) and does not occur in normal tissues (Fang et al. 2011; Maeda et al.
2016). Interestingly, in our recently published article, we demonstrated that fluores-
cently labeled fullerenes (C60-serPF) can be used as a model delivery system for bio-
distribution studies in a breast cancer model, due to their preferred biokinetic profile
(Lapin et al. 2017a).
Since their discovery in 1985, fullerene nanomaterials have drawn the attention of
medicinal chemists due to their unique biological properties (Nakamura and Isobe
2003). Over the last few decades, [60]fullerenes have been investigated for many bio-
medical applications, including targeted drug delivery, and as contrast agents and non-
viral transfection agents (Dellinger et al. 2013). The functionalization of the fullerene
cage with water solubilizing groups offers a versatile method for biological experiments,
as well as for conjugation with chemotherapeutic agents, fluorescent probes and cancer-
targeting antibodies (Zakharian et al. 2005; Ashcroft et al. 2006). Appropriately derivat-
ized [60]fullerene buckyballs become amphiphilic in nature with the ability to cross most
biological barriers, including the blood-brain barrier and nuclear membrane (Raoof
et al. 2012). Furthermore, fullerene nanomaterials are non-toxic even at high concen-
trations of up to 1 mg/mL (Serda et al. 2018). The anti-cancer activity of fullerenes has
mainly been described for in vivo models, where it has been explained by its ability to
inhibit tumor angiogenesis (metalloproteinases inhibitors) and its strong antioxidant
properties (Chen et al. 2005; Sun et al. 2016). Interestingly, it was described earlier
that water-soluble fullerene derivatives have the ability to resensitize cancer cells that
were previously resistant to cisplatin and doxorubicin (Zhang et al. 2009). The chemi-
cal functionalization of [60]fullerene using the cyclopropanation reaction, in which the
derivatives of malonic acid are particularly useful (Bingel-Hirsch reaction), offers novel
synthetic possibilities because it allows virtually any imaginable type of organic moiety
to be covalently linked to the carbon shell of hydrophobic [60]fullerene.
Pancreatic cancer is a highly lethal disease that has a 5-year survival rate of less than
10% (Siegel et al. 2015). Currently, the most successful treatment is the surgical resec-
tion of the tumor, but in many cases, it is not possible to perform the surgery because
only 20% of patients have resectable pancreatic cancer (Kamisawa et al. 2016). Thus, the
development of non-surgical treatments, including adjuvant therapy, is needed in order
to improve the prognosis for patients with pancreatic cancer. The first line of chemo-
therapeutic drugs that was used to treat pancreatic cancer was gemcitabine. The clinical
trials that have been performed have shown that patients with advanced pancreatic can-
cer have better survival rates and durations after treatment with gemcitabine compared
to those that were treated with 5-fluorouracil (Burris et al. 1997). Moreover, combina-
tions of gemcitabine and different chemotherapeutic agents as well as monoclonal anti-
bodies have also been studied for advanced breast cancer (Hu et al. 2015). Nevertheless,
the usefulness of the current strategies and the effects of gemcitabine monotherapy are

Nalepa et al. Cancer Nano
(2020) 11:2
Page 3 of 21
hampered by its chemo-resistance, low vascularization and drug biodistribution limita-
tions in the tumor microenvironment (Kleeff et al. 2007; Koay et al. 2014).
The use of nanoscale drugs that are designed to treat pancreatic tumors have been
widely explored in the last 5 years, which has resulted in Abraxane, a nano-formulation
of paclitaxel with albumin (Lee et al. 2013; Pan et al. 2015). Here, we report on a syn-
thetic protocol that enables a water-soluble [60]fullerene nanoconjugate with gemcit-
abine (called nanoC60GEM) to be generated.
### Materials and methods
Materials
All of the compounds that were used were reagent grade or better, and the solvents
were used as they were received unless otherwise specified. The following reagents were
used as received: C60 (99.5%, SES RESEARCH, USA), gemcitabine (Sigma Aldrich),
2-amino-1,3-propanediol (AK Scientific), DBU (1,8-diaza-bicyclo[5.4.0] undec-7-ene,
Sigma Aldrich), glycine (POCH, Poland), p-toluenesulfonic acid (POCH, Poland), ace-
tic anhydride (Acros Organics), malonic acid (Acros Organics), CBr4 (Sigma Aldrich),
EDCI hydrochloride [N-ethyl-N'-(3-dimethylaminopropyl)carbodiimide hydrochloride,
Acros Organics], N-hydroxysuccinimide (Sigma Aldrich) and sodium hydride (Acros
Organics). All of the solvents that were used to prepare the carbon nanomaterials were
prepared according to literature procedures by distilling them with calcium hydride
and were used immediately. The nuclear magnetic resonance spectra were measured
on a Bruker Avance III500 MHz NMR Spectrometer with TMS as the internal stand-
ard. The MS spectra for the water-insoluble fullerenes were collected using an Autoflex
II MALDI-TOF mass spectrometer, and for the water-soluble [60]fullerene derivatives
using an MS electrospray ionization time-of-flight (ESI-microTOF) mass spectrom-
eter, both instruments from Bruker Daltonics Inc (Fremont, CA, USA). The final dialy-
sis purification of the water-soluble nanomaterial nanoC60GEM was performed on Pall
Microsep™ centrifugal membranes with molecular cut-offs 1 and 3 kDa. The purity of all
of the compounds was assessed using an Agilent1260 equipped with a DAAD detector
at 260 nm, RP-column: Eclipse plus C18 (3,5 qm); flow 0.5 mL/min. The Fourier trans-
form infrared (FTIR) measurements were carried out using an Agilent Cary 640 FTIR
spectrometer equipped with a standard source and a DTGS Peltier-cooled detector. The
nanoconjugate powder was mixed with KBr and measured in the transmittance mode
in the 700-4000 cm-1 range. The spectrum was recorded at 32 accumulations with a
spectral resolution of 4 cm-1. The obtained data were analyzed by the baseline, water,
and carbon dioxide correction. The chemical analysis of the sample surface was per-
formed using X-ray photoelectron spectroscopy (XPS). The measurements were per-
formed on a PHI5700 Physical Electronics spectrometer. The XPS studies were carried
out with using an Al Ka monochromatized X-ray source (hv = 1486.6 eV). The survey
spectrum was measured at pass energy 187.75e eV, and the high-resolution core levels
of C1s, F1s, N1s, O1s and Si2 were measured at pass energy 23.5 eV. The analysis of
the chemical states of the detected elements, as well as the calculations of the atomic
concentration was performed using MULTIPAK (version 9.6.7.1, 2015, Ulvac-phi Inc.)
software. The near-infrared luminescence (1270 nm) was measured perpendicular to the
excitation beam in the photon-counting mode using a thermoelectric-cooled NIR PMT

Nalepa et al. Cancer Nano
(2020) 11:2
Page 4 of 21
module (H10330-45; Hamamatsu, Japan) equipped with a 1100 nm cut-off filter and an
additional dichroic narrow-band filter NBP, and was selectable from the spectral range
1150-1355 nm (NDC Infrared Engineering Ltd., Essex, UK). The data were collected
using a computer-mounted PCI-board multichannel scaler (NanoHarp 250; PicoQuant
GmbH, Berlin, Germany). Data analysis, including the first-order luminescence decay
fitted using the Levenberg-Marquardt algorithm, was performed by custom-written
software. The acquisition time for obtaining the singlet oxygen phosphorescence signals
was 20 s. The EPR measurements were taken using a Bruker EMX-AA EPR spectrom-
eter (Bruker BioSpin, Rheinstetten, Germany). EPR samples were run using microwave
power of 10.6 mW, a modulation amplitude of 0.05 mT, center field 339.0 mT, scan width
8 mT and scan time 21 s. The light for photodynamic therapy was delivered from royal
blue 100 W COB source (440 nm, FWHM 17.4 nm) (Chanzon, Shenzhen, China). The
cell plate was placed in a holder above light source. Distance from the lens was set to
achieve high uniformity of light power distribution on whole plate area. The cells were
irradiated with 20 mW/cm2 for 1000 s for a total dose of 20 J. Temperature of cells dur-
ing irradiation did not exceed 32 °C.
Methods
Synthesis of nanoC60GEM
2,2'-[(1,3-Dioxopropane-1,3-diyl)diimino]diacetic acid or malonyl-diglycine (1).
Glycine (9.75 g, 0.130 mol) was suspended in of 10 mL water and dissolved by adding
NaOH to the solution (5.21 g, 0.130 mol). A solution of diethyl malonate in 30 mL of
ethanol (10.4 g, 0.065 mol) was added and the whole mixture was placed in a 100-mL
flask and heated under reflux for 3 h. The solvent was then removed on a rotary evapo-
rator. Then, 12 M hydrochloric acid was being added to the residue until the pH of the
mixture reached 1. The flask with the mixture was placed in a refrigerator for 12 h; dur-
ing which the product precipitated. The resulting white solid was filtered off, washed
with cold water and ethanol and dried. The final product was obtained as a white solid
with a 19% yield (2.83 g) with m.p. 233 °C.
1H-NMR (dg-DMSO, 400 MHz, ppm): 8.35(t, J = 5.8 Hz, 2H, NH); 3.78(d, J = 5.8 Hz,
4H, CH2-NH); 3.17 (s, 2H, -CO-CH2-CO).
13C-NMR (d6-DMSO, 100 MHz, ppm): 171.5; 167.5; 42.9; 42.7; 41.2.
Diethyl 2,2'-[(1,3-dioxopropane-1,3-diyl)diimino]diacetate or diethyl malonyl-diglyci-
nate (2).
Compound 1 (8.00 g, 36.67 mmol) was dissolved in 150 mL of ethanol and 348.8 mg
(1.83 mmol, 5% molar ratio) of p-toluenesulfonic acid monohydrate was added. The
reaction mixture was heated under reflux for 90 h). The solvents were then removed on
a rotary evaporator to form solidifying oil. This product was purified using the extrac-
tion technique (DCM:NaHCO3 solution). The organic phase was dried using anhydrous
CaCl2 and evaporated in vacuo to form a slightly yellowish oil. The final product was
obtained with an 80% yield (8.09 g).
1H-NMR (dg-DMSO, 500 MHz, ppm): 8.44 (t, J = 5.7 Hz, 2H, NH);4.09 (m, 4H, CH2-
CH3); 3.85(d, J = 5.7 Hz, 4H, CH2-NH); 3.18(bs, 2H, -CO-CH2-CO); 1.18(t, J = 7 Hz,
6H, CH3).
13C-NMR (dg-DMSO, 125 MHz, ppm): 170.1; 167.6; 61.0; 42.9; 42.5; 41.3; 14.4, 14.3

Nalepa et al. Cancer Nano
(2020) 11:2
Page 5 of 21
Synthesis of diserinol malonate acetate (3)
Diserinol malonate and its peracetylated version were synthesized on a large scale
using a modified protocol (Serda et al. 2018). Briefly, 2-amino-1,3-propanediol (100 g,
1076 mmol) and dimethyl malonate (57.4 mL, 500 mmol) were dissolved in dry isopro-
panol, heated with vigorous stirring at 50 °C for 30 min and then stirred at room tem-
perature, under a nitrogen atmosphere for 14 days. After that time, the solid precipitate
was filtered off and washed with cold isopropanol. After recrystallization from isopro-
pyl alcohol, the white solid was obtained and dried under lyophilization (m.p. 132 °C,
yield 92%). Serinol malonate (25.0 g, 99.9 mmol) was suspended in pyridine (100 mL,
1240 mmol) at 0 °C, to which acetic anhydride (150 mL, 1590 mmol) was added drop-
wise over the course of an hour. After reaching 25 °C, dissolution occurred and the solu-
tion was stirred continuously for 48 h. At 0 °C, methanol (50 mL, 1225 mmol) was added
to quench the remaining acetic anhydride and the solution was stirred for 1 h, after
which the solvents were removed in vacuo and the residue (yellow oil) was dissolved
in dichloromethane and recrystallized for 12 h in hexane. The precipitate was collected
as white crystals via filtration, washed with hexane and dried in vacuo (m.p. 91 °C, lit.
91-92 °C (Clark et al. 1972)).
#### [60]Fullerene hexakis adduct (6)
The C60 (360 mg, 0.500 mol) was added to a freshly distilled toluene (400 mL), mixed
for 20 min using a magnetic stirrer and suspended using an ultrasonic bath. Then,
CBr4 (248.7 mg, 0.75 mmol) and malonate 2 (137.1 mg, 0.500 mmol), both of which
were suspended in dichloromethane (7 mL), were added. Next, 1,8-diazabicyclo[5.4.0]
undec-7-ene (DBU, 95.1 mg, 0.625 mmol) in 5 mL of DCM was added and the reac-
tion was allowed to proceed for 3 h at room temperature. The final product was isolated
using the flash chromatography technique, (silica: Mallinckrodt, 75-250 qm particles,
150 A pore size). The unreacted residue and impurities were removed with toluene and
dichloromethane and then the product was eluted with CH2Cl2:MeOH 5:1 (240 mL)
and CH2Cl2:MeOH 2:1 (225 mL) mixtures. The dark brown filtrate was evaporated in
vacuo to form a brown solid (powder). This final product was obtained with a 64% yield
(315 mg) and the mass was confirmed using MALDI-TOF (Additional file 1: Fig. S1). The
obtained monoadduct 4 (183 mg, 0.184 mmol), diserinol malonate acetate (771.1 mg,
1.843 mmol) and CBr4 (1222.3 mg, 3.686 mmol) were dissolved in 20 mL of DCM; to
which 170 mL of freshly distilled toluene was added and stirred for 5 min. Next, 1,8-diaz-
abicyclo[5.4.0]undec-7-ene (DBU, 337 mg, 2.212 mmol) in dichloromethane (3 mL) was
added slowly over the course of 4 h and the reaction was allowed to proceed with mix-
ing at room temperature for 34 h. Flash chromatography was used (silica: Mallinckrodt,
75-250 qm particles, 150 A pore size) to isolate the hexakis product. The unreacted resi-
due and some of the impurities were removed with toluene and dichloromethane and
then the product was eluted with a CH2Cl2:MeOH 5:1 (360 mL) mixture. The brown
filtrate was evaporated (100 mL flask) in vacuo to form a dark brown grease (2.003 g),
which was hydrolysed in order to obtain unprotected derivative 6. For this purpose, the
protected [60]fullerene derivative 5 (1.966 g) was dissolved in 20 mL of dry DCM and
then sodium hydride (200.0 mg, 8.33 mmol) was carefully added in portions and stirred

Nalepa et al. Cancer Nano
(2020) 11:2
Page 6 of 21
for 15 min. Next, methanol was added (8 mL, in portions of 0.2-0.5 mL) and during this
period, intense bubbling was observed (at the bottom of the flask, however, unreacted
so it remained). The flask was tightly closed and the reaction with mixing was allowed
to proceed at room temperature for 60 h. Then, 1.5 mL of methanol was added to the
brown mixture in the flask; no bubbling was observed. The solvents were evaporated
in vacuo to form a black solid (1.735 g). Next, a partially cleaved fullerene nanomaterial
was placed in a 100-mL flask and then 1,4-dioxane (18 mL) and concentrated hydro-
chloric acid (3 mL, 35%) were added (the black solid product immediately dissolved).
The flask was tightly closed and the reaction mixture was allowed to proceed for further
hydrolysis at room temperature for 7 days. The solvents were evaporated in vacuo to
form a brown solid of compound 6 (2.092 g). The final product was purified by dialy-
sis of an aqueous solution of fullerene 6 using cellulose membranes (molecular weight
exclusion limit 1.0 kDa; Spectrum Labs, USA). The dialysis lasted 7 days, and the final
fullerene nanomaterial 6 was concentrated, frozen and lyophilized. The final product
was obtained as a brown solid with a 35% yield (137.8 mg).
#### NanoC60GEM
In a small vial, 1-ethyl-3-(3-dimethylaminopropyl)carbodiimide (EDCI, 6.60 mg,
0.034 mmol), N-hydroxysuccinimide (NHS, 3.96 mg, 0.034 mmol) and fullerene 6
(30.0 mg, 0.0014 mmol) were dissolved in 2 mL of a MES buffer (10% 2-(N-morpholino)
ethanesulfonic acid in water, pH = 4.5). After 5 min of stirring, the whole mixture
was added (rinsing the vial twice with 0.5 mL of the MES buffer) into a reaction ves-
sel (10 mL) containing gemcitabine (GEM, 10.32 mg, 0.034 mmol). The [60]fullerene
derivative 6 was dissolved instantly and the reaction vessel was placed on a magnetic
stirrer at room temperature for 92 h. Afterwards, the final product was purified by dialy-
sis against an aqueous solution, using a cellulose membrane (10 mL, molecular weight
exclusion limit 1.0 kDa; Spectrum Labs, USA). The dialysis lasted 10 days and the water
was changed twice a day. Finally, the dialysate was concentrated, frozen and lyophilized.
The final product was obtained as a brown solid with a 79% yield (29.42 mg) and its
purity was confirmed by HPLC (Additional file 1: Fig. S7).
#### Time-resolved singlet oxygen detection
Phosphate-buffered (pD 7.4, 10 mmol) D2O solutions of nanoC60-GEM and TMPyP
in a 1-cm-optical path quartz fluorescence cuvette (QA-1000; Hellma, Mullheim, Ger-
many) was excited by light pulses that were generated by an integrated nanosecond DSS
Nd:YAG laser system, equipped with a narrow bandwidth optical parametric oscillator
(NT242-1k-SH/SFG; Ekspla, Vilnius, Lithuania). The laser system delivered pulses at
a 1-kHz repetition rate, with a pulse energy up to several hundred microjoules in the
visible region, and up to several tens of microjoules in the UVA-UVB region. The [60]
fullerene photosensitizers were photoexcited using a 427 nm wavelength. The absorb-
ance of the samples was set to 0.27 in that wavelength. In order to adjust the photoexci-
tation energy in the experiments, a laser beam was attenuated with three pieces of wire
mesh (light transmission 40% each). The quantum yield of singlet oxygen formation was
calculated using 5,10,15,20-tetrakis(1-methyl-4-pyridinio)porphyrin tetra(p-toluenesul-
fonate) (TMPyP) as the reference compound (ф = 0.75) (Snyder et al. 2006).

Nalepa et al. Cancer Nano
(2020) 11:2
Page 7 of 21
Electron paramagnetic resonance spin trapping studies
EPR spin trapping was used with DMPO as the spin trap at a concentration of
100 mM. Samples containing 0.1 mg/mL nanoC60GEM in 80% DMSO were irradiated
in EPR quartz flat cells in the resonant cavity with 402- to 508-nm (24 mW/cm2) light,
which was produced by a 300-W high-pressure compact arc xenon lamp (Cermax,
PE300CE13FM/Module300W; PerkinElmer Optoelectronics, GmbH, Wiesbaden,
Germany). The irradiation setup was equipped with a water filter, heat reflecting hot
mirror, cut-off filter that blocked light below 390 nm and a blue additive dichroic filter
505FD64-25 (Andover Corporation, Salem, NH, USA).
#### Cell lines and culture methods
The human breast carcinoma; MCF-7 and human lung carcinoma epithelial-like A549
were obtained from the American Type Culture Collection (ATCC). The human pan-
creas adenocarcinoma AsPc-1 and pancreatic carcinoma of a ductal origin PANC-1
were obtained from Sigma-Aldrich. The murine pancreatic ductal adenocarcinoma;
PAN02 was obtained from NCI-Frederick Cancer Research Facility and the normal
human fibroblasts NHDF was obtained from PromoCell. The cell lines; MCF-7, A549,
PANC-1 and NHDF were grown in Dulbecco’s modified Eagle’s medium (DMEM).
The DMEM for MCF-7, A549 and PANC-1 were supplemented with 12% heat-inac-
tivated fetal bovine serum (Sigma) and for the NHDF with 15% non-inactivated fetal
bovine serum (Sigma). The AsPc-1 and PAN02 cell lines were cultured in a RPMI
1640 medium (Gibco, UK), which had been supplemented with 10% heat-inacti-
vated fetal bovine serum (Sigma). All of the culture media were supplemented with
the antibiotics penicillin/streptomycin (Gibco) (1% v/v). The cell lines were grown as
monolayer cultures in 75 cm2 flasks (Nunc) under standard conditions at 37 °C in a
humidified atmosphere at 5% CO2. All of the cell lines were tested for Mycoplasma
contamination.
#### Cytotoxicity studies
The cells were seeded in 96-well plates (Nunc) at a density of 5 x 103 cells/well for the
cancer cell lines and 4 x 103 cells/well for the normal cell line (NHDF) and incubated
at 37 °C for 24 h. An MTS assay (CellTiter 96® AQueous One Solution Cell Prolifera-
tion Assay from Promega) was performed after a 72 h incubation of the cells using
nanoC60GEM (2-0.1 mg/mL) and gemcitabine (0.01-25 pM). The medium was then
removed and 20 mL of a CellTiter96®AQueousOne Solution-MTS (Promega) was added
to each well (with 100 mL DMEM without phenol red) and incubated at least for 1 h
at 37 °C. The absorbance of the samples was measured at 490 nm using a multi-plate
reader (Synergy 4, BioTek). The results which were expressed as a percentage of the con-
trol were calculated as the inhibitory concentration (IC50) values using GraphPad Prism
7. Each experiment was repeated at least three times, each in triplicate.
#### Cell cycle assay
The PAN02 cells were seeded in 3 cm Petri dishes (Nunc) at a density of 1.5 x 105
cells/dish and incubated at 37 °C for 24 h. Then, solutions of the nanoC60GEM (35

Nalepa et al. Cancer Nano
(2020) 11:2
Page 8 of 21
and 17 qM) and gemcitabine (1.5 and 0.75 qM) were added. After a 48-h treatment,
an assay was performed using a Muse Cell-Cycle Kit (Millipore) according to the
manufacturer’s instructions. Briefly, the cells were collected, washed with cold PBS
and centrifuged at 300g. Next, the cells were fixed in ice-cold 70% ethanol and stored
at — 20 °C overnight. Afterwards, the cells were centrifuged and resuspended in 200
qL of a Muse™ Cell Cycle Reagent and incubated for 30 min at room temperature in
the dark. After staining, the cells were processed for the cell cycle analysis using a
Muse Cell Analyzer (Millipore). The experiments were performed at least three times,
each in triplicate.
#### Annexin V binding assay
The PAN02 cells were seeded in 3-cm Petri dishes (Nunc) at a density of 1,5 x 105 cells/
dish and incubated at 37 °C for 24 h. Then, solutions of the nanoC60GEM (35 and 17 qM)
and gemcitabine (1.5 and 0.75 qM) were added. After 48 h, an assay was performed
using an Annexin V & Dead Cell Kit (Millipore) according to the manufacturer’s instruc-
tions. Briefly, both detached and adherent cells were collected and centrifuged at 500 g
for 5 min. Afterwards, the resuspended cells were incubated with 100 qL of a Muse™
Annexin V & Dead Cell Reagent for 20 min at room temperature in the dark. After
staining, the events for live, early and late apoptotic cells were counted using a Muse
Cell Analyzer (Millipore). The experiments were performed at least three times, each in
triplicate.
#### Photodynamic therapy on the PAN02 cell line
The PAN02 line cells were plated in 24-well plates at density of 35,000/well. Twenty-four
hours after plating, the cells were incubated with high-glucose DMEM that contained
nanoC60GEM at different concentrations. Feeding was repeated two more times, at 24-h
intervals. The day after the final feeding the cells were washed twice with PBS that con-
tained calcium and magnesium ions, then irradiated for 15 min using a blue led light
(440 nm) at a fluence rate 20 mW/cm2. Dark control cells were kept in the same condi-
tions except light exposure. After irradiation, the cells were provided with DMEM with
10% FBS. The cytotoxic effect of the photodynamic treatment was quantified 24 h after
irradiation, using a MTT assay for the mitochondrial redox function. The MTT solution
in DMEM with 10% FBS was added to the treated and control culture wells (final con-
centration of 0.5 mg/mL). After incubation for 30 min at 37 °C, the culture medium was
removed and the remaining blue precipitate was solubilized in DMSO, followed by read-
ing the absorbance at 560 nm in a plate reader (GENios Plus, Tecan Austria GmbH). The
results are reported as the percentage of the paired untreated controls. The experiments
were repeated a minimum of three times.
#### Statistical analysis
The results are expressed as the mean ± standard deviation (SD) from at least three inde-
pendent experiments. A statistical analysis was performed using the one-way ANOVA
with a Bonferroni post hoc test. A p value of 0.05 or less was considered to be statisti-
cally significant. GraphPad Prism v.7.0 software (GraphPad Software, USA) was used for
the analysis (Fig. 1).

Nalepa et al. Cancer Nano
(2020) 11:2
Page 9 of 21
Fig. 1 Chemical structure of nanoC60-GEM
Results and discussion
Synthetic protocol and characterization of nanoC60GEM
The synthetic protocol for obtaining nanoC60GEM is shown in Scheme 1. During our
design step, we decided to use a glycine derivative of malonic acid 1 as the substrate for
the Bingel-Hirsch reaction. We expected that the carboxylic groups, which are present
in that compound would be much more reactive toward the aromatic amines (i.e., the
cytosine fragment in the gemcitabine) in contrast to the malonic acid derivatives, which
are closely connected the [60]fullerene scaffold, based on literature findings (Wang et al.
2015). The desired [60]fullerene monoadduct 4 was created in a high yield by in situ gen-
eration of a-brominated malonate 2 in the presence of CBr4/DBU at room temperature
in a time-controlled reaction, where monoadducts were formed up to 3 h. However,
after that time, bis- and tris-adducts formed, which made the purification process more
complicated. The structure of the monoadduct 4 was confirmed using MALDI-TOF
spectrometry with a characteristic peak at 992 Da and no presence of the bis- or tris-
adducts (Additional file 1: Fig. S1). The second Bingel-Hirsh reaction was performed
using diserinol malonate acetate (malonate 3) in order to ensure a high degree of water
solubility and the desired hexakis adduct with Th symmetry was created (compound 5)
in a good yield. The deprotection of fullerene 5 was performed in a two-step procedure,
which involved hydrogenolysis with sodium hydride first and then the final hydrolysis
with 1,4-dioxane with concentrated HCl added. The molecular peak of the [60]fullerene
derivative 6 is shown in Additional file 1: Fig. S2 with the characteristic mass of 2195 Da
[M + H2O + H]+ and no signals from the pentakis isomer. The final step of the conjuga-
tion with GEM was performed using the water-soluble carbodiimide EDCI/NHS sys-
tem in a solution of a MES buffer. The ESI spectrometry confirmed the formation of the
desired nanoC60GEM (Additional file 1: Fig. S3) which had a characteristic signal of the
molecular peak at 2690 Da [M + Na]+, which represented the [60]fullerene derivative 6
that had been conjugated to two molecules of gemcitabine via an amide bond. Interest-
ingly, a fragmentation pattern, in which one serinol group left the nanoC60GEM (charac-
teristic at 2578 Da, Additional file 1: Fig. S3), was observed.
The UV-VIS spectrum of nanoC60GEM is characteristic for the water-soluble fuller-
enes that have a high absorbance only in the UV and blue regions of a spectrum (max
absorbance was observed at 220 nm). Moreover, we found that nanoC60GEM tends to
form monodisperse aggregates around 120 nm as was confirmed by DLS (Additional

Nalepa et al. Cancer Nano
(2020) 11:2
Page 10 of 21
Scheme 1 Synthetic pathway for obtaining nanoC60GEM
file 1: Fig. S4), and which may be disintegrated into smaller individual fullerenes inside
the cell (Lapin et al. 2017b). The zeta potential measurements of our gemcitabine nano-
conjugate (Additional file 1: Fig. S5) also indicated a surface charge of — 25 mV, thus con-
firming a relatively good degree of stability.
The infrared spectrum of the nanoC60GEM system was divided into two spectral
regions: (1) 2700-3800 cm-1 and (2) 700-1850 cm-1 (Fig. 2). The high wavenum-
ber region is characterized by the presence of a broadened band that is centered at
3364 cm-1, which corresponded to the overlapping signal that had originated from the

Nalepa et al. Cancer Nano (2020) 11:2	Page	11	of	21
hydroxyl (Motoyama and Jarboe 1966) and the secondary amide vibration (Lumley Jones
1963). The observable band shift toward a lower wavenumber, especially in relation to
the hydroxyl group, may have resulted from the formation of an inter- or intramolecular
hydrogen bonding scheme. In turn, the low-wavenumber bands with their maxima cen-
tered at 2927 and 2841 cm-1 may have originated from the asymmetric and symmetric
stretching mode of the methylene groups that overlapped with the stretching vibration
of the CH moieties.
The fingerprint (1) region, especially at high wavenumbers with a maxima located at
1790, 1724 and 1678 cm-1, is determined by the carbonyl stretching modes due to pri-
mary amides (Craig and Evans 1965). The deformational mode of the secondary amide
could have corresponded to the band at 1535 cm-1. In addition, this band has a combi-
nation character with vibration originated from the medium-strong vibration within the
furan (Katritzky and Lagowski 1959) as well as the C=C and C=N ring stretching vibra-
tions within the pyrimidin-2-one (Billes et al. 1998). The other low-intense bands with
their maxima at 1371 and 1248 cm-1 were mainly linked to the deformational modes
of the methylene groups that were located within the aliphatic chain or the furan and
pyrimidin-2-one rings. In turn, the interpretation of the band at 1048 cm-1 was unam-
biguous because of the overlapping character of the various modes that may be acti-
vated at this wavenumber such as a C=C-H deformation within the aliphatic moieties
or within the furan and pyrimidin-2-one, the CN of a secondary amine or asymmetric
and symmetric vibration of the CF. In turn, the deformational mode of the CF could
have been expected at 726 cm-1. Finally, one can summarize that the band arrangement
indicated on the presence of the hydroxyl, secondary amine, and fluorine substituents,
which confirmed that the synthesis had been performed successfully.
The chemical states of the elements that were present on a sample surface were
analyzed using XPS. The change in the binding energy was related to changes in the
chemical bonding with the surrounding elements. An analysis of the carbon chemical
states was performed to analyze the C1s core level. A resolved line, see Fig. 3a, indi-
cates the presence of several different chemical states of the carbon. The state with
the lowest binding energy of 282.84 eV was associated with the presence of an impu-
rity of an SiC origin. The amount of this state was relatively low about 4.19% of the
entire amount of carbon (see Additional file 1: Table S1). The highest peak, which
Fig. 2 a Infrared spectrum of nanoconjugate measured in the 700-4000 cm 1 range. b UV-VIS spectrum of
nanoC60GEM recorded in ultrapure water (c = 0.01 mg/mL)
V

Nalepa et al. Cancer Nano (2020) 11:2	Page	12	of	21
Fig. 3 The XPS high-resolution photoemission lines of nanoC60-GEM: a carbon C1s, and b fluorine FIs
was located at 284.71 eV, indicates the presence of C-C and C-H type bonds (Watts
1993). The peak centered at 286.33 eV could be assigned to the C-O and C-N bonds
and has been the case for other fullerene derivatives (Yu et al. 2012), whereas the peak
at 287.74 eV corresponds to the states that have been observed in poly(vinyl fluoride)
(Clark et al. 1973) or fluorobenzene (Clark et al. 1972) compounds. Fluorine analy-
sis was difficult, mainly due to the quality of the spectrum, which resulted from the
small amount of this element in the sample. Calculations of the atomic concentration
indicated about 0.06 atomic percent of F on the sample surface, which is generally the
detection limit of the XPS technique.
Nevertheless the fluorine 1s photoemission line had (see Fig. 3b) a peak that was
located at 687.63 eV, and similar values were observed for graphite fluorides for which
the peaks located in the range of 687-689 eV were assigned to the adsorbed fluorine
(Palchan et al. 1989). The weakly developed peak at 687.63 eV may be associated with
polyvinylidene fluoride (PVDF); however, as this state represents only 7% of all of the
fluorine, which is itself a trace element, the analysis could not be precise. An analysis
of oxygen confirmed what had been observed in the C1s C-O bonds. For nitrogen,
the N1s line indicated the presence of two chemical states, one weakly developed at
397.57 eV, which was related to the Si3N4 compound and the second of high intensity

Nalepa et al. Cancer Nano (2020) 11:2	Page	13	of	21
at 399.78 eV, which was related to the bonds that present in nylon. In the case of sili-
cone, two chemical states were also present, one was centered at 100.33 eV and was
related to SiC and the second at 102.02 eV, which was related to Si3N4. Additionally,
a small amount of bromine was observed and was associated with AgBr. Taking into
account the atomic concentrations, which were calculated from the XPS measure-
ments, in which the amount of carbon was approximately 79.39 at.%, oxygen 15.36
at.%, nitrogen 3.89 at.%, fluorine 0.06 at.%, silicone 1.14 at.%, and bromine 0.15 at.%,
both the Si and Br can be treated as trace elements that appeared due to synthetic
impurities or sample preparation.
#### Biophysical characterization of nanoC60GEM
The water-soluble [60]fullerene nanomaterials are well-known for their ability to pro-
duce different types of reactive oxygen species when irradiated by blue light (Mroz et al.
2007).
Based on previous literature studies, in polar solvents, in particular those contain-
ing donor electrons such as NADH, the irradiation of fullerenes leads to the generation
of reduced oxygen species, such as superoxide anion radical (O2-) and hydroxyl radi-
cal (OH«). In non-polar solvents such as benzene, the process of singlet oxygen (3O2) is
primarily formed (Yamakoshi et al. 2003). UV light has a very low ability to penetrate
through tissue and can cause a non-specific effect in any cells it hits. In our study, we
used blue LED light, which has a slightly better tissue penetration that does not cause
any damage to cells that have no photosensitizer. The photoreactivity of the analyzed
fullerene nanoparticles was determined by measuring their ability to generate, after irra-
diation with blue LED light, singlet oxygen and superoxide anion, which may have oxi-
dizing effects on several cellular targets, especially under conditions with a low-oxygen
concentration. In this study, we carried out singlet oxygen photogeneration studies of
nanoC60GEM using a cationic porphyrin (TMPyP) as the reference photosensitizer.
The calculated quantum efficiency of 3O2 formation for our water-soluble [60]fullerene
derivative, which had been irradiated by blue LED light was around 0.05. Although the
efficacy of singlet oxygen formation for pristine fullerene is almost at unity (at 532 nm),
chemical modifications can decrease their efficacy (Arbogast et al. 1991). Earlier stud-
ies with Bingel-Hirsch products confirmed the observation that monoadducts as well
as aminofullerenes produce singlet oxygen more effectively than hexakis adducts (as
nanoC60GEM) (Hamblin 2018). More importantly, we discovered that in the presence of
bovine serum albumin (100 mM) this process is reduced, suggesting a close interaction
between fullerene and the formation of the protein corona (Fig. 4c).
We also measured superoxide photogeneration using the EPR spin-trapping method
with DMPO as the spin trap. While nanoC60GEM alone showed a negligible signal of
trapped adducts, the presence of electron donor (NADH) increased the signal by an
order of magnitude (Fig. 4b), thus showing that in favorable conditions, the electron
transfer route may also contribute to a phototoxic effect. Spin trapping was performed
in 80% DMSO, which made any measurements in the presence of BSA impossible as it
would have destroyed the protein structure. Although the photoreactivity of our novel
fullerene nanomaterial is not very high, its localization within cancer cells could make it
more phototoxic if it is localized, for example, in the nucleus (Serda et al. 2018).

Nalepa et al. Cancer Nano
(2020) 11:2
Page 14 of 21
Fig. 4 Photoreactivity of nanoC60GEM. a Quantum yield of singlet oxygen generation after irradiation by
blue LED light by nanoC60GEM with TMPyP used as the reference photosensitizer; b spin adduct signal
(DMPO-OOH) that was formed in the absence and presence of an electron donor (0.5 mM NADH) after blue
LED light irradiation; c 1270 nm luminescence observed in the absence and presence (100 |jM) of bovine
serum albumin

Nalepa et al. Cancer Nano
(2020) 11:2
Page 15 of 21
Biology
Cytotoxicity
We performed cytotoxicity screening using several cancer cell lines of different origins
including normal human fibroblasts. During the biological studies, we decided to study
pancreatic, breast and lung cancers because of the clinical use of GEM for the aforemen-
tioned neoplasms (Xie et al. 2018; Watanabe et al. 2019). The calculated IC50 values are
presented in Table 1.
We observed a noticeable cytotoxicity for two cell lines, MCF-7 and PAN02, for which
we calculated the I C50 parameters to be 2.07 ± 0.64 and 7.35 ± 1.13 qM, respectively.
Compared to gemcitabine alone, the cytotoxic effect was reduced. A possible expla-
nation of this phenomenon may be the ineffective transport of nanoC60GEM into the
nucleus. Gemcitabine is a deoxycytidine analog with two additional fluoride atoms and
as nucleoside derivative, it is transported throughout human nucleoside transporters
(hNTs) (Mackey et al. 1998).
We hypothesized that after GEM was conjugated with [60]fullerene, this type of trans-
port would be unavailable. Additionally, GEM is incorporated into the C60 structure
by the formation of an amide bond which, for steric hindrance, is probably difficult to
access through the cellular enzymes such as proteases. Despite its higher activity toward
the MCF-7 cell line, we selected the PAN02 cell line for the further studies because we
also wanted to perform in vivo studies.
Cell cycle
In order to evaluate the mechanism of action of nanoC60GEM, we performed a flow
cytometry measurement. As is presented in Fig. 5, after 48 h of the incubation with
nanoC60GEM and gemcitabine, we observed a decrease in the faction of cells in the G0/
G1 phase (compared to the control). However, there was an increase in the number of
cells in the S phase in all of the cases that were examined regardless of the concentration.
This increase indicated an inhibition of the cell cycle in the S phase. This is consistent
with Huang’s studies for gemcitabine (Huang et al. 1991), which indicates that it inhibits
DNA synthesis. After its uptake into a cell, gemcitabine is metabolized into an active
triphosphate form. Thereafter, this form is embedded in the DNA chain, thereby pre-
venting its elongation.
Cell death
In order to determinate the type of the cell death, we also used flow cytometry. In this
experiment, after 48 h of incubation with nanoC60GEM and gemcitabine, we measured
the green signal that was derived from apoptotic cells. As is presented in Fig. 6, the
Table 1 Antiproliferative activity of the studied compounds
Compound	IC50 ImM]
	MCF-7	AsPc-1	PAN02	PANC-1	A549	NHDF
NanoC60GEM	2.07 ± 0.64	> 375	7.35 ± 1.13	> 375	> 375	> 375
Gemcitabine	0.044 ± 0.008	0.207 ± 0.046	0.027 ± 0.003	21.95 ± 3.99	> 25	> 25

The IC50 parameters were calculated using GraphPad Prism 7

Nalepa et al. Cancer Nano
(2020) 11:2
Page 16 of 21
biggest fraction of the apoptotic cell was detected for gemcitabine (44% compared to
the control). There was no big difference between the two concentrations of GEM (0.75
and 1.5 qM) that were tested. However, for nanoC60GEM, we also registered a compa-
rable population of apoptotic cells (38.6% for 35 qM of nanoC60GEM). These results are
promising from the perspective of further studies.
Phototoxicity studies
According to research reports, [60]fullerene derivatives have a great potential
to be used as photosensitizers in photodynamic therapy. In order to evaluate this
hypothesis, we performed experiments in which the cells were incubated with
nanoC60GEM for 3 days to cause the cellular nucleases to cleave GEM from the
nanoconjugate, after which the cells were irradiated with blue LED light. After the
Fig. 5 Effect of the tested nanoC60GEM (35 and 17 pM) and GEM (1.5 and 0.75 pM) on regulating the cell
cycle in the PAN02 cell line. The histograms show the distribution of the cells in the G0/G1, S and G2/M
phases of the cell cycle for an exemplary experiment (a). The table shows the mean ± SD percentage of the
cells in the G0/G1, S and G2/M phases of the cell cycle from three independent experiments (b). The data
were analyzed using a one-way ANOVA with a Bonferroni's post hoc test: *p < 0.05, **p < 0.01, ***p < 0.001
compared to the control (c)
X

Nalepa et al. Cancer Nano
(2020) 11:2
Page 17 of 21
Fig. 6 Evaluation of the induction of apoptosis in the PAN02 cell line after a 48-h treatment with
nanoC60GEM (35 and 17 jM) and GEM (1.5 and 0.75 jM). The histograms show the percentage of early and
late apoptosis for one of the experiments (a). The table shows the mean ± SD percentage of the live, early
and late apoptotic cells from three independent experiments (b). The data were analyzed using one-way
ANOVA with a Bonferroni's post hoc test: *p < 0.05, **p < 0.01, ***p < 0.001 compared to the control (c)
irradiation a cell viability assay was performed (24 h, MTT). The selection of the
correct wavelength (440 nm) to be used was dictated by the absorption properties
of the studied nanomaterial (Fig. 2b), in order to avoid UV part of the spectrum that
could cause unspecific effects. As is depicted in Additional file 1: Fig. S4, the tested

Nalepa et al. Cancer Nano
(2020) 11:2
Page 18 of 21
compound did not generate a significant level of the singlet oxygen and superoxide
anion. Addition of an electron donor increased the superoxide production many-
fold (Fig. 4b), but such favorable conditions are difficult to find in a cellular envi-
ronment. Therefore, we conducted the experiments by adding BSA (Fig. 4c), which
confirmed the interaction of the fullerene nanomaterial and the formation of the
protein corona. Our results show that the interaction with conducts serum protein
leads to a decrease in the observable signal of singlet oxygen, which may be caused
by a decreased yield of the generation or by an increased quenching of the singlet
oxygen by bounded proteins. To explore this issue in depth, we performed in vitro
studies using a medium that contained FBS. The results, which are presented in
Fig. 7, confirmed the non-toxic properties of the low concentrations of irradiated
nanoC60GEM, which reduced the chances of using this type of fullerene nanomate-
rial as a photosensitizer. Although the PAN02 cell line phototoxicity response was
disappointing, we plan to study the effects of nanoC60GEM on different cancer cell
lines and 3D-spheroids.
conclusions
The developed synthetic protocol was able to produce a highly water-soluble
[60]fullerene nanoconjugate with gemcitabine in good yield. The physio-chemi-
cal characteristics of the fullerene nanomaterial confirms that two gemcitabine
units are attached to the [60]fullerene scaffold via formation of amide bonds. The
nanoC60GEM cytotoxicity effect was dependent on its concentration in PAN02 cells,
but its phototoxic effects were mild, partly due to the formation of the protein corona
on the surface of the [60]fullerene scaffold as well as the low quantum yields of the
singlet oxygen generation. Further biological studies using 3D-spheroids as well as
murine models should be used in order to evaluate the efficacy of a therapy using
nanoC60GEM.
Fig. 7 Phototoxicity of nanoC60GEM performed for the PAN02 cancer cell line

Nalepa et al. Cancer Nano
(2020) 11:2
Page 19 of 21
### Supplementary information
Supplementary information accompanies this paper at https://doi.org/10.1186/s 12645-020-00058-4.
Additional file 1. The physico-chemical characteristics of nanocC60GEM.
Abbreviations
ATCC: American Type Culture Collection; BSA: Bovine serum albumin; DLS: Dynamic light scattering; DMEM: Dulbecco's
modified Eagle medium; DBU: 1,8-Diaza-bicyclo[5.4.0]undec-7-ene; DCM: Dichloromethane; DMPO: 5,5-Dimethyl-
1 -pyrroline N-oxide; DMSO: Dimethylsulfoxide; DNA: Deoxyribonucleic acid; EDCI: 1 -Ethyl-3-(3-dimethylamino propyl)
carbodiimide; EPR: Enhanced permeability and retention effect; EPR: Electron paramagnetic resonance; FBS: Fetal bovine
serum; FDA: Food and Drug Administration; GEM: Gemcitabine; IC50: Half-maximal inhibitory concentration; LED: Light
emitting diode; MALDI: Matrix-assisted laser desorption/ionization; jM: Micromolar; MS: Mass spectrometry; MTT: (3-
[4,5-Dimethyl-thiazol-2-yl]-2,5-diphenyltetrazolium bromide); NADH: Nicotinamide adenine dinucleotide reduced form;
nanoC60GEM: [60]Fullerene derivative nanoconjugate with gemcitabine; NHS: N-Hydroxysuccinimide; PBS: Phosphate-
buffered saline; PVDF: Polyvinylidene fluoride; RPMI: Roswell Park Memorial Institute; S phase: Synthesis phase; TMPyP:
5,10,15,20-Tetrakis(1-methyl-4-pyridinio)porphyrin tetra(p-toluenesulfonate); XPS: X-ray photoelectron spectroscopy.
Acknowledgements
Not applicable.
Authors' contributions
Conception and design: MS, GSZ and AMW. Acquisition of data: PN, RG, GS, MS, KB, MD, and MS. Analysis and interpreta-
tion of the data: MS, GSZ and AMW. Manuscript preparation: MS, GSZ, AMW, JP and RM wrote the manuscript. All authors
read and approved the final manuscript.
Funding
Dr. Maciej Serda thanks the National Science Center (Poland) for its support (Grant SONATA UMO-2016/23/D/
NZ7/00912). Dr. Mateusz Dulski is thankful for the financial support from the National Science Center based on decision
2017/26/D/ST8/01117.
Availability of data and materials
The datasets used and/or analyzed during the current study are available from the corresponding author on reasonable
request.
Ethics approval and consent to participate
Not applicable.
Consent for publication
Not applicable.
Competing interests
We confirm that we have given due consideration to the protection of intellectual property associated with this work
and that there are no impediments to publication, including the timing of publication, with respect to intellectual prop-
erty. The authors declare that they have no competing interests.
Author details
1 Institute of Chemistry, University of Silesia in Katowice, Katowice, Poland. 2 Institute of Physics and Silesian Center
for Education and Interdisciplinary Research, University of Silesia in Katowice, Katowice, Poland. 3 Faculty of Biochemistry,
Biophysics and Biotechnology, Jagiellonian University, Kraków, Poland. 4 Institute of Materials Engineering and Silesian
Center for Education and Interdisciplinary Research, University of Silesia in Katowice, Katowice, Poland.
Received: 5 October 2019 Accepted: 3 February 2020
Published online: 18 February 2020
References
Arbogast JW, Darmanyan AP, Foote CS, Diederich FN, Whetten RL, Rubin Y, Alvarez MM, Anz SJ. Photophysical properties
of sixty atom carbon molecule (C60). J Phys Chem. 1991;95(1):11-2.
Ashcroft JM, Tsyboulski DA, Hartman KB, Zakharian TY, Marks JW, Weisman RB, Rosenblum MG, Wilson LJ. Fullerene (C60)
immunoconjugates: interaction of water-soluble C60 derivatives with the murine anti-gp240 melanoma antibody.
Chem Commun. 2006;28:3004-6.
Billes F, Mikosch H, Holly S. A comparative study on the vibrational spectroscopy of pyridazine, pyrimidine and pyrazine. J
Mol Struct (Thoechem). 1998;423(3):225-34.
Burris HA 3rd, Moore MJ, Andersen J, Green MR, Rothenberg ML, Modiano MR, Cripps MC, Portenoy RK, Storniolo AM,
Tarassoff P, et al. Improvements in survival and clinical benefit with gemcitabine as first-line therapy for patients with
advanced pancreas cancer: a randomized trial. J Clin Oncol. 1997;15(6):2403-13.
Chen C, Xing G, Wang J, Zhao Y, Li B, Tang J, Jia G, Wang T, Sun J, Xing L, et al. Multihydroxylated [Gd@C82(OH)22]n nano-
particles: antineoplastic activity of high efficiency and low toxicity. Nano Lett. 2005;5(10):2050-7.
Chow EK, Ho D. Cancer nanomedicine: from drug delivery to imaging. Sci Transl Med. 2013;5(216):216rv214.

Nalepa et al. Cancer Nano
(2020) 11:2
Page 20 of 21
Clark DT, Kilcast D, Adams DB, Musgrave WKR. An ESCA study of the molecular core binding energies of the fluoroben-
zenes. J Electron Spectrosc Relat Phenom. 1972;1(3):227-50.
Clark D, Feast W, Kilcast D, Musgrave W. Applications of ESCA to polymer chemistry. III. Structures and bonding in
homopolymers of ethylene and the fluoroethylenes and determination of the compositions of fluoro copolymers. J
Polym Sci. 1973;11(2):389-411.
Craig NC, Evans DA. Infrared and Raman Spectra of cis- and trans-1,2-dichloro-1,2-difluoroethylene. J Am Chem Soc.
1965;87(19):4223-30.
Dawidczyk CM, Kim C, Park JH, Russell LM, Lee KH, Pomper MG, Searson PC. State-of-the-art in design rules for drug deliv-
ery platforms: lessons learned from FDA-approved nanomedicines. J Control Release. 2014;187:133-44.
Dellinger A, Zhou Z, Connor J, Madhankumar AB, Pamujula S, Sayes CM, Kepley CL. Application of fullerenes in nano-
medicine: an update. Nanomedicine. 2013;8(7):1191-208.
Fang J, Nakamura H, Maeda H. The EPR effect: unique features of tumor blood vessels for drug delivery, factors involved,
and limitations and augmentation of the effect. Adv Drug Deliv Rev. 2011;63(3):136-51.
Hamblin MR. Fullerenes as photosensitizers in photodynamic therapy: pros and cons. Photochem Photobiol Sci.
2018;17(11):1515-33.
Hu X-C, Zhang J, Xu B-H, Cai L, Ragaz J, Wang Z-H, Wang B-Y, Teng Y-E, Tong Z-S, Pan Y-Y, et al. Cisplatin plus gemcitabine
versus paclitaxel plus gemcitabine as first-line therapy for metastatic triple-negative breast cancer (CBCSG006): a
randomised, open-label, multicentre, phase 3 trial. Lancet Oncol. 2015;16(4):436-46.
Huang P, Chubb S, Hertel LW, Grindey GB, Plunkett W. Action of 2;, 2/-difluorodeoxycytidine on DNA synthesis. Cancer
Res. 1991;51(22):6110-7.
Kamisawa T, Wood LD, Itoi T, Takaori K. Pancreatic cancer. Lancet. 2016;388(10039):73-85.
Katritzky A, Lagowski J: 130. Infrared absorption of heteroaromatic, five-membered, monocyclic nuclei. Part I. 2-Mono-
substituted furans. Journal of the Chemical Society (Resumed) 1959:657-660.
Kim BY, Rutka JT, Chan WC. Nanomedicine. N Engl J Med. 2010;363(25):2434-43.
Kleeff J, Beckhove P, Esposito I, Herzig S, Huber PE, Lohr JM, Friess H. Pancreatic cancer microenvironment. Int J Cancer.
2007;121(4):699-705.
Koay EJ, Baio FE, Ondari A, Truty MJ, Cristini V, Thomas RM, Chen R, Chatterjee D, Kang Y, Zhang J, et al. Intra-tumoral het-
erogeneity of gemcitabine delivery and mass transport in human pancreatic cancer. Phys Biol. 2014;11(6):065002.
Lapin NA, Krzykawska-Serda M, Dilliard S, Mackeyev Y, Serda M, Wilson LJ, Curley SA, Corr SJ. The effects of non-invasive
radiofrequency electric field hyperthermia on biotransport and biodistribution of fluorescent [60]fullerene deriva-
tive in a murine orthotopic model of breast adenocarcinoma. J Control Release. 2017a;260:92-9.
Lapin NA, Vergara LA, Mackeyev Y, Newton JM, Dilliard SA, Wilson LJ, Curley SA, Serda RE. Biotransport kinetics and intra-
tumoral biodistribution of malonodiserinolamide-derivatized [60]fullerene in a murine model of breast adenocarci-
noma. Int J Nanomed. 2017b;12:8289-307.
Lee GY, Qian WP, Wang L, Wang YA, Staley CA, Satpathy M, Nie S, Mao H, Yang L. Theranostic nanoparticles with controlled
release of gemcitabine for targeted therapy and MRI of pancreatic cancer. ACS Nano. 2013;7(3):2078-89.
Lumley Jones R. The infrared spectra of some simple N-substituted amides in the vapor state. J Mol Spectrosc.
1963;11(1):411-21.
Mackey JR, Mani RS, Selner M, Mowles D, Young JD, Belt JA, Crawford CR, Cass CE. Functional nucleoside transporters are
required for gemcitabine influx and manifestation of toxicity in cancer cell lines. Cancer Res. 1998;58(19):4349-57.
Maeda H, Tsukigawa K, Fang J. A retrospective 30 years after discovery of the enhanced permeability and retention
effect of solid tumors: next-generation chemotherapeutics and photodynamic therapy—problems, solutions, and
prospects. Microcirculation. 2016;23(3):173-82.
Motoyama I, Jarboe CH. Hydroxyl Group Stretching Frequency and Extinction Coefficient Studies on Aliphatic Alcohols.
The Journal of Physical Chemistry. 1966;70(10):3226-8.
Mroz P, Pawlak A, Satti M, Lee H, Wharton T, Gali H, Sarna T, Hamblin MR. Functionalized fullerenes mediate photodynamic
killing of cancer cells: type I versus Type II photochemical mechanism. Free Radical Biol Med. 2007;43(5):711-9.
Nakamura E, Isobe H. Functionalized fullerenes in water. the first 10 years of their chemistry, biology, and nanoscience.
Acc Chem Res. 2003;36(11):807-15.
Palchan I, Crespin M, Estrade-Szwarckopf H, Rousseau B. Graphite fluorides: an XPS study of a new type of C-F bonding.
Chem Phys Lett. 1989;157(4):321-7.
Pan Y, Wang L, Kang SG, Lu Y, Yang Z, Huynh T, Chen C, Zhou R, Guo M, Zhao Y. Gd-metallofullerenol nanomaterial sup-
presses pancreatic cancer metastasis by inhibiting the interaction of histone deacetylase 1 and metastasis-associ-
ated protein 1. ACS Nano. 2015;9(7):6826-36.
Raoof M, Mackeyev Y, Cheney MA, Wilson LJ, Curley SA. Internalization of C60 fullerenes into cancer cells with accumula-
tion in the nucleus via the nuclear pore complex. Biomaterials. 2012;33(10):2952-60.
Serda M, Ware MJ, Newton JM, Sachdeva S, Krzykawska-Serda M, Nguyen L, Law J, Anderson AO, Curley SA, Wilson LJ,
et al. Development of photoactive Sweet-C60 for pancreatic cancer stellate cell therapy. Nanomedicine (Lond).
2018;13(23):2981-93.
Siegel RL, Miller KD, Jemal A. Cancer statistics, 2015. CA Cancer J Clin. 2015;65(1):5-29.
Snyder JW, Lambert JD, Ogilby PR. 5, 10, 15, 20-tetrakis (N-Methyl-4-Pyridyl)-21 H, 23H-porphine (TMPyP) as a sensitizer
for singlet oxygen imaging in cells: characterizing the irradiation-dependent behavior of TMPyP in a single cell.
Photochem Photobiol. 2006;82(1):177-84.
Sun C, Wang L, Gao D, Pan Y, Zhao Y, Chen C, Guo M. C60(OH)22: a potential histone deacetylase inhibitor with anti-
angiogenic activity. Nanoscale. 2016;8(36):16332-9.
Wang L, Zhu X, Tang X, Wu C, Zhou Z, Sun C, Deng S-L, Ai H, Gao J. A multiple gadolinium complex decorated fullerene
as a highly sensitive T 1 contrast agent. Chem Commun. 2015;51(21):4390-3.
Watanabe S, Yoshioka H, Sakai H, Hotta K, Takenoyama M, Yamada K, Sugawara S, Takiguchi Y, Hosomi Y, Tomii K. Necitu-
mumab plus gemcitabine and cisplatin versus gemcitabine and cisplatin alone as first-line treatment for stage IV
squamous non-small cell lung cancer: a phase 1b and randomized, open-label, multicenter, phase 2 trial in Japan.
Lung Cancer. 2019;129:55-62.

Nalepa et al. Cancer Nano
(2020) 11:2
Page 21 of 21
Watts JF. High resolution XPS of organic polymers: the Scienta ESCA 300 database. G. Beamson and D. Briggs. 280 pp.,£
65. John Wiley & Sons, Chichester, ISBN 0471 935921,(1992). Surf Interface Anal. 1993;20(3):267.
Xie Z, Zhang Y, Jin C, Fu D. Gemcitabine-based chemotherapy as a viable option for treatment of advanced breast cancer
patients: a meta-analysis and literature review. Oncotarget. 2018;9(6):7148.
Yamakoshi Y, Umezawa N, Ryu A, Arakane K, Miyata N, Goda Y, Masumizu T, Nagano T. Active oxygen species generated
from photoexcited fullerene (C60) as potential medicines: O2-* versus 1O2. J Am Chem Soc. 2003;125(42):12803-9.
Yu J, Guan M, Li F, Zhang Z, Wang C, Shu C, Wei H, Zhang X-E. Effects of fullerene derivatives on bioluminescence and
application for protease detection. Chem Commun. 2012;48(89):11011-3.
Zakharian TY, Seryshev A, Sitharaman B, Gilbert BE, Knight V, Wilson LJ. A fullerene — paclitaxel chemotherapeutic: synthe-
sis, characterization, and study of biological activity in tissue culture. J Am Chem Soc. 2005;127(36):12508-9.
Zhang Q, Yang W, Man N, Zheng F, Shen Y, Sun K, Li Y, Wen L-P. Autophagy-mediated chemosensitization in cancer cells
by fullerene C60 nanocrystal. Autophagy. 2009;5(8):1107-17.
Publisher's Note
Springer Nature remains neutral with regard to jurisdictional claims in published maps and institutional affiliations.
Ready to submit your research? Choose BMC and benefit from:
- fast, convenient online submission
- thorough peer review by experienced researchers in your field
- rapid publication on acceptance
- support for research data, including large and complex data types
- gold Open Access which fosters wider collaboration and increased citations
- maximum visibility for your research: over 100M website views per year
At BMC, research is always in progress.
Learn more biomedcentral.com/submissions