Hindawi Publishing CorporationJournal of Spectroscopy
Volume2013,ArticleID187407,8pageshttp://dx.doi.org/10.1155/2013/187407
Research Article
SpectroscopicandGasChromatographicStudiesofPigments and Binders in GdaNsk Paintings of the 17thCentury
Justyna Olszewska-Uwietlik,1Bohena Szmelter-Fausek,1Ewa Piwta,2and Edyta Proniewicz2,3
1DepartmentofPaintingTechnologiesandTechniques,NicolausCopernicusUniversityinTorun´,UlicaSienkiewicza30/32,87-100Torun´,Poland
2FacultyofChemistry,JagiellonianUniversity,UlicaIngardena3,30-060Krako´w,Poland
3Faculty of Foundry Engineering, AGH University of Science and Technology, Ulica Reymonta 23, 30-059 Krakow, Poland
CorrespondenceshouldbeaddressedtoJustynaOlszewska-S´wietlik;justyna.olszewska-swietlik@umk.plReceived 5 September 2013; Accepted 30 October 2013
Academic Editor: Yizhuang Xu
Copyright©2013JustynaOlszewska-S´wietliketal.ThisisanopenaccessarticledistributedundertheCreativeCommonsAttributionLicense,whichpermitsunrestricteduse,distribution,andreproductioninanymedium,providedtheoriginalworkisproperlycited.
Thisworkpresentsspectroscopic(opticalmicroscopy,OM;micro-Raman,Raman;andFourier-transformadsorptioninfrared,FT-IR)andgaschromatographicstudiesoftwofamouspanelpaintingsfromtheGdan´skartistsofthe17thcenturyGoldenAge,
⋅
“ServiliusAppius”byIsaacvandenBlockeand“AllegoryofWealth”probablybyAntonMo¨ller.Applicationoftheaforementioned
(2PbCO⋅
methods allowed us to identify pigments and binders used in the panel paintings. In particular, it was determined that the
2
yellowpigmentusedbybothartistsislead-tinyellowtypeI(2PbO
SnO),thewhitepigmentislead(II)carbonatehydroxide
3
2
3
Pb(OH)),andthegroundlayermaterialconsistofchalk(CaCO).Theanalysisshowedalsothatinthecaseof“Allegory
ofWealth,”theredlayerconsistsnotonlyofcinnabar(HgS)butalsooflead-tinyellowtypeI.
⋅
2 3
3	32
2
2	3
2	3
2
1. Introduction
Several documentary sources from the 17th century give recipes on how to paint, prepare grounds, and use colors for particular parts of the painting [1–4].Forexample, De Mayernepronouncedthatthequalityofthematerialsused isessentialnotonlyforthegroundlayerbutalsoforthepaintlayer.Herecommended putting two different groundlayers
ironoxidered[FeO],naturalazurite[Cu(CO)(OH)],
smalte [CoO
nKSiO],naturalmalachite[CuCO(OH)],
3
2
coppergreen[Cu(CHCOO)],andcharcoalwerethemost
common pigments used in the 17th century [8]. Massicot
[PbO],schu¨ttgelb(yellowlakepigment—organicpigments
2 3
frommanydifferentsources),andorpiment[AsS]werealso
mentionedinthedocumentarysourcesfromthisperiod[1–
4].However,thelaterliteraturenotedthatlead-tinyellowwasincorrectlyidentifiedasmassicot[9,10].Forexample,DeMayernesuggestedusingmassicot(infactlead-tinyellow),yellowochre,andschu¨ttgelbtopaintlightedandshadedsurfaces,aswellastransitionfromlighttoshade[1–4].
on the support. The first ground layer consisted of a very
3
asecondlayeroflead(II)carbonatehydroxide[(PbCO)⋅
thinchalk-glue[CaCO—awhitepigmentusedasapainting
3 2
groundsinceantiquity[5]]thathepolished.Then,heapplied
2
Pb
umber [Fe O⋅
(OH)—asyntheticpigmentproducedsinceantiquityusing
Despite
progress
in
the field of instrumental analysis,
23	2
2 3
anacidicorganiccompoundonmetalliclead[6,7]with
identificationofsomeofthepigmentspresentinthepainting
(typeII)—Pb(Sn,Si)O],yellowochre[FeO⋅
HO+MgO+AlO][1].Lead(II)carbonate
2	4
layers,especiallylead-tinyellow,isnotalwaysasimpletask.Dependingonthemethodofpreparation,twotypesoflead-tinyellowcanbeobtained(typeIandtypeII).
Recipes for lead-tin yellow are given in the Bolognese
hydroxide,lead-tinyellow[light(type1)—PbSnOanddark
3
23	2
HO],vermil-
ion[HgS,asyntheticequivalentofcinnabar[8]],redlead
3 4
PaperSegreti per colorifrom the XVth century: “272.
To
[minimum, Pb O ], carmine (organic red—carminic acid),

2
Journal of Spectroscopy
make yellow glass for paternosters or beads.Takeof lead1lb.,oftin2lbs.,meltandcalcinethem,andmakeglassforpaternosters.”and “273.Tomake giallolino forpainting.Take2lbs.ofthiscalcinedleadandtin,thatis2lbs.ofthisglassforpaternosters,2.5lbs.ofminimum,and0.5lb.ofsandfromVald’Arnopoundedveryfine;putitintoafurnaceandlet itfineitselfandthecolorwillbeperfect”[11].Accordingto adifferentrecipe,lead-tinyellowwasobtainedbyheatingapproximately3partsoftheoxide,leaddioxide,ormostoftenminiumwith1partoftinoxide[10,12–14].
Lead-tinyellowtypeIoccursmorefrequentlyinartthandoeslead-tinyellowtypeII.Thispigmentwaswidely applied from antiquity to the first half of the 18thcentury[15].ItsearlyusewascharacteristicinNorthernEurope.However,from the second half of theXVthcentury,itwas identifiedinpaintingsfromseveralEuropeanschools.Forexample,lead-tinyellowtypeIwasfoundinthepaintingsoftheNetherlandishartistsMasteroftheSaintBartholomew(1475–1510) and Gerard David (1460–1523), the Flemish artistAnthonyvanDyck(1599–1641),andtheDutchartistsHendrick ter Brugghen (1588–1629) and Meindert Hobbema(1638–1709),whoseworksareintheNationalGalleryinLondon [7]. In works from the Polish collections, lead-tin yellowtypeI,intraceamounts,wasidentifiedintheDutchtriptych“TheLastJudgement”(1473)byHansMemling(1435–1494)(theNationalMuseuminGdan´sk)[16].
Lead-tin yellow type II was obtained from lead glass, according to the procedure given in the Bolognese Paper [10,12–14].Thistypeofyellowwasusedmoreofteninthe southernschoolsofpainting,andtheearliestexamplewas identifiedinthepaintingsofGiottodiBondone(1266–1377) andJacopodiCione(1325–1399)[7].InthesecondhalfoftheXVthcenturyinItaly,lead-tinyellowtypeIIwasreplacedbylead-tinyellowtypeI[7].ExamplesincludeworksbyMorettoda Brescia (1498–1555) and PaoloVeronese(1528–1588) fromthecollectionsoftheNationalGalleryinLondon,inwhich lead-tinyellowtypeIwasidentifiedbyX-RayDiffractionanalysis[16].
Duringthe16thand17thcenturies,Gdan´skwasawealthyseaport and merchantcity.Manyartists, including immi-grantsfromtheNetherlands,livedinGdan´skandcomposedtheirworksofartthatinfluencedthenativeGdan´skartists.OneofthefamiliesthatsettledinGdan´skwasthevandenBlockefamilyfromMechelen(Flanders).Theytookup construction,ornamentalmasonry,andpainting.IsaacvandenBlockewasapainterandgainedareputationasasplendidartistfortheMainTownHallinGdan´sk(1606–1609)[17].
ThesecondoutstandingGdan´skartistisAntonMo¨ller,
2
1
Figure1:“ServiliusAppius”(1608-1609)byIsaacvandenBlocke andacross-sectionofsample(SA):SA.1—whitegroundlayer/un-derpaintingandSA.2—yellowpaintinglayer.
3
2
1
Figure2:“AllegoryofWealth”(c.1600)byAntonMo¨llerandacross-sectionofsample(AW):AW.1—whitegroundlayer/under- painting,AW.2—redpaintinglayer,andAW.3—yellowpaintinglayer.
who
arrived
in
Gdan´skfromKro´lewiec.Mo¨ller’sartwas
influenced by Netherlandish and German painters. His
Appius”byIsaacvandenBlocke(Figure1)and“AllegoryofWealth,”mostlikelybyAntonMo¨ller(Figure2).Thisworkis important because the examination of the type of lead- tinyellowinagreaternumberofpaintingswillcontribute toafullviewofthetechnologiesandtechniquesthatwere usedandthetypesofmaterialsinthepaintingsindifferent regionsofEurope.Thesecondgoaloftheresearchwasto gain analytical information on the inorganic and organicmaterialsusedforgrounds,paintinglayers,andvarnishesinbothpaintingstobetterunderstandandcharacterizetheir
famous work is “The Last Judgement” (1602-1603) fromArthusCourtinGdan´sk.
Both artists are best known for Biblical themesandallegoricalcompositionsthatareoftencomparedtotheartofFlandersandtheNetherlands.
Themainaimoftheanalysispresentedinthisworkwastosupplementthedataonthetypeoflead-tinyellowpigmentusedintheGdan´skpaintingsinthefirsthalfoftheXVIIthcentury,usingthetwoexamplepaintings“Servilius

Journal of Spectroscopy
3
−1
paintingtechnique.Itwasimportanttoidentifythepigments, howcomplexthebindingmediamixturesusedforthelayerswere,andifthepaintingsshowanycharacteristicfeaturesrelatedtocertainschoolsofpainting.Theobtaineddatawerealsoimportanttobetterplanthesustainableconservationof thepaintings.ThepresentresearchisthefirstspectroscopicinvestigationoftheGdan´sk17thcenturypaintings.Untilnow,theGdan´sk17thcenturypaintingshavebeenstudiedonlybyarthistorians.
“ServiliusAppius”(1608-1609) was painted for theRedChamberintheMainTownHallinGdan´sk(nowTheGdan´skHistoryMuseum).IsaacvandenBlockeplacedmoreemphasisonthepoliticalandadministrativecontentofthispaintingthanonitsartisticvalue.Thethemeofthepainting was directed to the city council and warnedagainstconflicts.Itemphasizescooperationasanimportantvirtue for governance [18]. Blocke mainly used yellow colors inparticularpartsofgarments,thatis,collarsandclothing finishing.
“AllegoryofWealth”(1600)ispartofanallegoricalcycle,alongwiththetwopaintingsknownas“TheModeloftheWorldandtheGdan´skCitizens”and“AllegoryofPride.”ThepaintingspointoutvicesofthecitizensofGdan´sk.Theauthormainlypaintedwithyellowcolorindetailsuchasshoesorornamentalsonthetextilesofrobes.
A multidisciplinary approach was undertaken to accom- plish these goals. Optical microscopy (OM), gas chromatog-raphy(GC),Fourier-transformabsorptioninfrared(FT-IR), and micro-Raman (Raman) analysis answered questions regardingthetypeoflead-tinyellowortheparticularpig-mentsandbindersusedinpaintingsofthistype.
rangeof4000–500cm	(JadwigaW.Łukaszewicz,Wiesława
Topolska,DepartmentforConservationandRestorationof Architectonic Elements and Details, The Institute for theStudy,RestorationandConservationofCulturalHeritage,NicolausCopernicusUniversityinTorun´,Poland).
2.5. GasChromatographyMeasurements.Samples weredecomposedtoseparatebindersonthecolumn.First,a2MmethanolicKOHsolutionwasused,followedbymethylation with methyl chloroformate (MCF) and the hexane extractionof methyl esters of saturated fatty acids and dicarboxylicacids such as azelaicacid.
Forthesemeasurements,aHewlettPackard6890Chro-matographequippedwitha30mHP5capillarycolumnandflameionizationdetectorFIDwasused.Theseparation was performed in a programmable temperature furnace (GrzegorzJaworski,Department of PaintingTechnologiesandTechniques,TheInstitutefortheStudy,RestorationandConservationofCulturalHeritage,NicolausCopernicusUniversityinTorun´,Poland).
The obtained chromatograms were interpreted qualita-tively by comparing the chromatograms of the referencebinder,such as linseed oil and casein.Fromthe chro-matogram integration results, the ratios between acids weredetermined,thatis,Az/Pa,Pa/St,andPa/My,whereAz,Pa,
St,
and My denote
azelaic,
palmitic, stearic, and
myristic
acids,respectively.Unfortunately,duetothesmallamountof
sampletakenfromthepainting“AllegoryofWealth,”itwas not possible to measure the binding media of theselected layersintheAWsample.Consequently,themeasurementswereperformedonasamplethatincludedalllayers.
BeforetheGCanalysiswasperformed,acomplementarymicrochemicalsaponificationtestwasperformedwiththe samplestoverifythepresenceofoilintheparticularlayers.
1. Materials andMethods
  1. Samples.Twosamplesweretakenfromyellowpartsofthepaintings:theyellowvestfrom“ServiliusAppius”byIsaacvandenBlocke(SA)andtheyellowshoefrom“AllegoryofWealth”byAntonMo¨ller(AW).Thecross-sectionswerepreparedbysettingthesamplesinresinandpolishingthesample.
1. Results andDiscussion
  1. VibrationalAnalysis.Analysisofacross-sectionofSA (insetinFigure1)andAW(insetinFigure2)samplesbyoptical microscopy and micro-Raman spectroscopy (Figures3and4)revealedthatthesamplesaremultilayeredandhave twoandthreelayers,respectively.TheSAsampleconsistedofthefollowinglayers:SA.1—whitegroundlayer/underpaintingandSA.2—yellowpaintinglayer(seeTable1);incontrast,theAWsample displayed the following layers:AW.1—whiteground layer/underpainting,AW.2—redpaintinglayer,andAW.3—yellowpaintinglayer(seeTable1).EachRamanspectrumfromtheindividualcross-sectionshowsunique bandsduetoparticularpigments.Thespectralanalysisofthesebandswasbasedonthespectraldatabasesofpigments[19–40].
2.2. Optical Microscopy Measurements.OM measurements werecarriedoutusingaNikonOptiphot-2(NIKONINC.,USA)conventionalreflectedlightmicroscope.
2.3.Micro-RamanMeasurements.The micro-Raman spectraofselectedlayerswererecordedusinganInViaspectrometer(Renishaw,England). This spectrometer was equippedwith
adiodelaseremittingat785.0nmandaCCDdetector.The
−1
laserpowerattheoutputwassetat30mW.Allspectrawere
−1
acquiredwithaspectralresolutionof4cm	in the 100to
3200cmspectralrange.Dependinguponthesignaltonoise
RamananalysisoftheSA.1layer(Figure3)identifieda
−1
ratio(S/N),4to16scanswerecollected.
mixtureofpigmentsinthislayerthatyieldaspectrumwith
−1
strongbandsfromchalk(at1087and278cm)andlead
2.4.Fourier-TransformAbsorption InfraredMeasurements.TheFT-IRspectraofSAandAWsamples(ground,under- painting,paintinglayer,andvarnish)wereobtainedwitha BrukerOpticsAlphaATRFTIRspectrometerinthespectral
(II)carbonatehydroxide(at1054cm).Thepresenceoflead
(II)carbonatehydroxideintheSA.1layerisaconsequence
of mixing the ground layer with the very thin layer ofunderpainting. The Raman spectrum of the yellow painting

4
Journal of Spectroscopy
Table1:Stratigraphyandresultsofthemeasurementsofpigmentsandbindersofacross-sectionoftheSAandAWsamples.
AW.1—whiteground layer/
underpainting
Detected pigments and binders
No.
Layer
Micro-Raman
FT-IR
GC
SA
⋅
Yellowpaintinglayer
Lead-tin
Oil, protein,carbonates
Linseedoil
AW.2—redpainting layer
2
yellow typeI
(2PbO
SnO )
2
chalk (CaCO3),
white groundlayer/underpainting
lead(II)
Linseedoil,casein
(2PbCO⋅
1
carbonate
hydroxide
Pb(OH) )
3
2
AW.3—yellowpainting layer
AW
⋅
Yellowpaintinglayer
Red paintinglayer
White groundlayer/underpainting
Lead-tin
Linseedoil,casein
3
yellow typeI
Casein
(2PbO
SnO2),
Cinnabar
2
1800 1600 1400 12001000800	600	400	200
Wavenumbers (cm−1)
Figure4:Micro-Ramanspectraofthecross-sectionlayersof“Al-legory ofWealth”(AW).
(HgS)
Chalk(CaCO),
Casein, gluten glue,carbonates
3
(2PbCO⋅
lead(II)carbonate
1
hydroxide
Pb(OH) )
3
2
resultsaremostlikelyduetocontaminationofthesampleduringembeddingintheresinblockordisplacementofsomegrainsofthesepigmentsfromthepreviouspaintinglayer.TheOMandmicrochemicalanalysesrevealedchalk, charcoal,andleadwhiteintheAW.1layer.Theredpaintinglayer(Figure4,AW.2layer)alsocontainsvermilion,asisevidentfromthepresenceofthesamespectralfeaturesas mentionedinthepreviouscases(layerAW.1).Similartothe
SA.1—white ground layer/
underpainting
RamanspectrumoftheSA.2layer,theAW.3layerspectrum
−1
SA.2—yellow paintinglayer
exhibitedbandsthatcorrespondedtolead-tinyellowtypeI
contain Raman band at∼137cm	which could notbe
(at127,195,272,291,454,and524cm).
−1
ItshouldalsobenotedthatbothSA.1andAW.1spectra
uniquelyassignedtoanyofpigments.Thisisduetothe
factthattherearenoadditionalobservedspectralfeatures.
Consequently,we could only suppose that this Raman signalarising from the lead tin yellow type I or II.
Theidentificationofvarnishesandbindingmediais oneofthemostcomplicatedissuesforscientistsandartconservators.ThechemicalcompositionofthesematerialsshouldbeanalyzedusingspectroscopicandchromatographictechniquessuchasFT-IRandGC.Figure5presentstheFT-IRspectraofthesamplefromtheinvestigatedpanelpaintings,whereasFigure6showstheirGCchromatograms.ThebindingmediaidentifiedintheSAandAWsamplesbasedontheFT-IRspectraarelinseedoilandprotein[20,23]. Hence,theobservedfattyacidsandesterbandsintheFT-
1800 1600 1400 12001000 800	600	400	200
Wavenumbers (cm−1)
Figure3:Micro-Ramanspectraofthecross-sectionlayersof“Ser-viliusAppius”(SA).
layer(Figure3,SA.2layer)exhibitedaprominent129,spectral
−1
feature,andlessintensebandsat195,272,291,454,and
522cm.Allofthesebandswereattributedtolead-tinyellow
typeI.
TheRamanspectrumoftheAW.1layer(Figure4),similar
totheRamanspectrumoftheSA.1layer,ischaracterized
IRspectramaybeexplainedbytheuseofdryingoilsin
−1
−1
−1
bybandsduetothemixtureofpigments,suchaschalk(at
thepreparationofthebinder.Briefly,intheIRspectraof
−1
alcoholic groups in the analyzed samples. The∼2926 and
1088cm),lead(II)carbonatehydroxide(at1052cm),and
the SA andAWsamples (Figure5), the3349cm	band
duetotheO–Hbondstretchrevealsthepresenceofthe
redpigmentcinnabar(vermilion,at252,282,and342cm).
−1
Duetothehistoricalcontextoftheart,bandsattributedto
cinnabar should not be observed in theAW.1layer.These
2855cm	spectralfeaturescorrespondtotheC–Hbond
Raman Intensity
10541087
522
454
291
278
272
195
129
137
Raman intensity
1088
1052
454
343
342
291
284
196
253
252
272
195
136
129
127

Journal of Spectroscopy
5
SA
AW
500
1000
1500
2000
2500
3000
Wavenumbers(cm−1)
Figure5:FT-IRspectraofsampletakenfrom“ServiliusAppius”(SA)and“AllegoryofWealth”(AW).
−1
stretchesofthehydrocarbonchains(fattyacidsandproteins).
AW(Figure6,bottomtrace)samplesindicatethefollowingacids: palmitic—Pa, stearic—St,myristic—My,and azelaic— Az.Fromtheresultsoftheintegrationofthechromatograms, theratiosbetweentheacidscanbedetermined(Pa/St,Az/Pa,Pa/My,Pa—palmitic, St—stearic, Az—azelaic, andMy—myristic).TheratiosofthepaintinglayertotheSAsampleareassignabletolinseedoil:Pa/St=1,92,Az/Pa=0,26,andPa/My
=10,37.ThepresenceofthisbinderwasconfirmedbyGCandFTIRanalysisandthemicrochemicaltest.Thesaponificationtestalsoconfirmedthepresenceofoil.
Forthe ground layer with underpainting, theratios werePa/St=2,28,Az/Pa=0,19,andPa/My=5,64,whichsuggeststhatthebindercompositionismostlikelycaseinandlinseedoil.ThisresultwasalsoconfirmedbyFT-IRanalysis.TheGCanalysisofthepaintinglayerswiththeground
−1
Thebroadintensebandwithamaximumat1708cm	and
ashoulderat1658cm	is due to the stretchingvibrations
2
of the C=O groups of resin acids and the C=CH olefin
−1
groups,respectively.Oils and proteins are represented by
−1
thecharacteristic1448cm	band (deformations of C–Hin
2
3
∼1170,and∼1090cm	spectralfeaturessuggestthepresence
–CH–and–CHgroups),whereasthe878and674cm
−1
Ramansignalsareonlyassignabletolinseedoil.The1245,
ofanestergroup.Theproteinmediaasananimalgluealso
−1
−1
showscharacteristicproteinvibrations,suchastheamideI
−1
(1658cm)andamideII(1549cm)bandsandthearomatic
−1
aminoacidsringmodes(1514,1605cm).Inthefingerprint
spectralregion,the1448,1378,1164,1094,and1057cm
bands may indicate the presence of a triterpenoid resinof
of the
AW
sample
assigned
the following
ratios: Pa/St=
dammar.Inaddition,chalkexhibitstypicalcalciumcarbon-
4,10,Pa/My=3,92,andAz/Pa=0,46,indicatingthatthebindercompositionismostlikelylinseedoilandcasein.The
−2
−1
atebandssuchastheantisymmetricstretchingvibrationof
3
CO	(1416and710cm).Thepresenceofthecarbonate
microchemicaltestofsaponificationofthesampleconfirmedthepresenceofoilinthepaintinglayerandunderpainting. TheFT-IRanalysisalsoconfirmedtheanalyzedbinders.
TheGCchromatogramoftheSAsample(Figure6,top trace)confirmedtheresultsoftheFT-IRanalysis(Figure5, toptrace)andrevealedlinseedoilinthepaintinglayerwithunderpaintingandcaseinandlinseedoilinthegroundlayer.
bandssuggeststheexistenceofcalciumcarbonateboundwith
calciteinthegroundlayerandlead(II)carbonatehydroxideinthepaintinglayerandtheunderpainting.
The type of binding medium used in the investigatedpanelpaintingswasalsodeterminedusinggaschromatogra-phy.ThechromatogramsoftheSA(Figure6,toptrace)and
Absorbance
607
1054
1057
10910176
1094
1164
1244
1448
1708
1400
1448
1708
2855
2855
2920
2926

6
Journal of Spectroscopy
SA
180
160
140
120
100
80
60
40
20
Pa
St
Az
My
0
2
4
6
8
10
t(min)
12
14
16
18
AW
90
80
70
60
50
40
30
20
0
2
4
6
8	10
t(min)
12
14
16
18
Figure6:GCchromatogramof“ServiliusAppius”(SA)(theintegrationofthepeakscalculatedratiosofacids:Pa/St=1,92;Az/Pa=0,26;Pa/My= 10,37; Pa—palmitic acid, St—stearic acid, Az—azelaic acid, and My—myristic acid) and“AllegoryofWealth”(AW)(the integrationofthepeakscalculatedratiosofacids:Pa/St=4,10;Pa/My=3,92;Az/Pa=0,38).
ThepresenceofcaseinandlinseedoilwasalsofoundintheAWsample(Figure6,bottomtrace),whichwasconfirmedbyFT-IRanalysis(Figure5,bottomtrace).
Appius,”whereaschalk,lead(II)carbonatehydroxide,lead- tinyellowI,andcinnabar(vermilion)wereusedin“AllegoryofWealth.”Blockepaintedwithoilcolorsonawhiteground that contained chalk and casein and on an underpaintingoflead(II)carbonatehydroxideandlinseedoil.Heusedlead-tinyellowtypeIasayellowpigment.Mo¨llerpaintedwithoilcolorsonawhitechalk-glue-caseingroundandan underpainting of lead (II) carbonate hydroxide was thenapplied.Theyellowlayercontaininglead-tinyellowtypeIwasappliedtoaredlayerofcinnabar(vermilion).
FTIRandGCidentifiedthecompositionofthebindingmedia.Theresultswerecompletedbymicro-Ramananalysis.TheobtainedresultshavebeencomparedwiththeFT-
IRdata(Figure5).Duetothesmallamountofsample,it wasnotpossibletoobtainFT-IRspectrafromeachlayer.ThecombinationofRSandFT-IRspectroscopyprovedtobecomplementaryintheidentificationofpigments.
Thevibrationalanalysisofthetwopanelpaintingsshowsthatartistsofthisperiodwerefamiliarwithusingpigmentssuchaslead-tinyellowtypeIorlead(II)carbonatehydroxide and the same ground layer material chalk. Thesesimilarities
4. Conclusions
The analyzed paint samples originated from the panel
paintings “Servilius Appius”
and “Allegory ofWealth.”An
interdisciplinary approach was used for the investigation ofthese samples to obtain information about their complex structureandtogainknowledgeofthetraditionalpainting techniquesandtherelatedtechnologicalsources.TheOM,
micro-Raman,FT-IR,andGCanalyticaltechniques,which characterize all of the usual classes of inorganicpigmentsandorganicbindingmediafromthesamemicrosamplewereused.Theanalysisofthebinderwasnecessarytocharacterizethepaintingandplanitsconsolidation.
Theperformedanalysisidentifieddifferencesbetween thetechniquesused.Forexample,chalk,lead(II)carbonatehydroxide,andlead-tinyellowtypeIwereusedin“Servilius
pA
pA
1.527
1.881
1.666
2.202
2.4242.109
1.719
2.9612.024
2.891
2.876
3.182
3.890
4.932
6.181
7.569
8.440
7.517
8.406
9.800
8.681
8.715
10.620
11.643
12.416
10.606
11.639
12.409
12.625
12.633
13.355
13.572
14.260
14.470
14.481
16.181

Journal of Spectroscopy
7
suggestthatbothofthesepaintingswerecreatedundertheinfluenceofthesameschoolorculture.
1. Z.Kaszowska,AdvantagesandLimitationsofAnalyticalTech-niquesUsedinTechnologicalStudiesofGothicPanelPaintings,WKiRDSASP,Krako´w,Poland,2010.
2. A.Deneckere,M.Leeflang,M.Bloemetal.,“Theuseofmobile Raman spectroscopy to compare three full-page miniatures fromthebreviaryofArnoldofEgmond,”SpectrochimicaActaA,vol.83,no.1,pp.194–199,2011.
3. K. Higgitt, M. Spring, andD.Saunders,Pigment-MediumInteractionsinOilPaintFilmsContainingRedLeadorLead-Tin- Yellow,vol.24,NationalGalleryTechnicalBulletin,2003.
4. J.Tylicki,TheNetherlandsOriginofthevandenBlockeFamily,vol.71,BiuletynHistoriiSztuki,2009.
5. J.Pałubicki,Gdan´skPainters.Painters,Glaziers,GraphicArtists,andEngraversinModernGdan´skArchivalMaterials,vol.2,TheNationalMuseuminGdan´sk,Gdan´sk,Poland,2009.
6. T.Grzybkowska,AureaPortaoftheRepublicofPoland,vol.2,TheNationalMuseuminGdan´sk,Gdan´sk,Poland,1997.
7. P.Vandenabeele,B.Wehling,L.Moens,H.Edwards,M.de Reu,andG.vanHooydonk,“Analysiswithmicro-Ramanspectroscopyofnaturalorganicbindingmediaandvarnishesusedinart,”AnalyticaChimicaActa,vol.407,no.1-2,pp.261– 274,2000.
8. M.Abdel-Ghani,H.G.M.Edwards,B.Stern,andR.Janaway,“CharacterizationofpaintandvarnishonamedievalCoptic- Byzantineicon:novelusageofdammarresin,”SpectrochimicaActaA,vol.73,no.3,pp.566–575,2009.
9. P.Vandenabeele,M.Ortega-Avile`s,D.T.Castilleros,andL.Moens, “Raman spectroscopic analysis of Mexican natural artists’materials,”SpectrochimicaActaA,vol.68,no.4,pp.1085–1088,2007.
10. C.Daher,C.Paris,A.-S.leHoˆ,L.Bellot-Gurlet,andJ.-P.E´chard,“AjointuseofRamanandinfraredspectroscopiesfortheidentificationofnaturalorganicmediausedinancientvarnishes,”JournalofRamanSpectroscopy,vol.41,no.11,pp. 1494–1499,2010.
11. L.BurgioandR.J.H.Clark,“LibraryofFT-Ramanspectraof pigments, minerals, pigment media and varnishes, and supplementtoexistinglibraryofRamanspectraofpigments withvisibleexcitation,”SpectrochimicaActaA,vol.57,no.7,pp.1491–1521,2001.
Conflict of Interests
Theauthorsdeclarethatthereisnoconflictofinterests regardingthepublicationofthepaper.
Acknowledgment
This work was supported by the Polish National ScienceCenteroftheMinistryofScienceandHigherEducation(Grantno.NN204370340toJ.O.-S´.).
References
1. T.T.deMayerne,“Pictoria,sculptoria,tinctoriaetquaesubal-ternarumatriumspectantia,”inQuellenfu¨rMaltechnikwa¨hrendderRenaissanceundderenFolgezeit(XVI.XVIII.Jahrhundert)in Italien, Spanien, den Niederlanden, Deutschland,Frankreichund England,nebstdemdeMayerneManuskript,E.Berger,Ed.,p.98,Callwey,Mu¨nchen,Germany,1901.
2. C.vanManderandH.Floerke,DasLebenderniederla¨ndischenunddeutschenMaler,vol.2,GeorgeMu¨ller,Mu¨nchen,Ger-many,1906.
3. C.vanMander,HetSchilder-Boeck,MartinusNijhoffPublishers,TheHague,TheNetherlands,1916.
4. M.Roznerska,PaintingsTechniquesof“SmallNetherlandsMas-ters”ofXVIICentury,NicolausCopernicusUniversity,Torun´,Poland,1991.
5. I. M. Bell, R.J.H. Clark,P.J.Gibbs, and Christopher Ingold Laboratories,Raman Spectroscopic Library ofNat-uraland Synthetic Pigments, University College London,Department of Chemistry, 2010,http://www.chem.ucl.ac.uk/resources/raman/index.html.
6. T.D.Chaplin, R.J.H. Clark, A.McKay,and S. Pugh,“Ramanspectroscopicanalysisofselectedastronomicaland cartographicfoliosfromtheearly13thcenturyIslamic‘Book ofCuriositiesoftheSciencesandMarvelsfortheEyes’,”JournalofRamanSpectroscopy,vol.37,no.8,pp.865–877,2006.
7. N. Eastaugh,V.Walsh,T.D.Chaplin, and R. Siddall,ThePigment Compendium: A Dictionary of Historical Pigments, ElsevierScience,Oxford,UK,2004.
8. J.Olszewska-S´wietlik,PaintingTechnologyandTechniqueofSelectedModernEpitaphsfromtheSt.Mary’sChurchinGdan´sk,NicolausCopernicusUniversity,Torun´,Poland,2009.
9. R.Jacobi,“U¨berdeninderMalereiverwendetengelbenFarbstoffderaltenMeister,”AngewandteChemie,vol.54,pp.28–29,1941.
10. H.Ku¨hn,“Lead-tin-yellow,”StudiesinConservation,vol.13,pp.7–33,1968.
11. M.Merrifield,OriginalTreatisesontheArtsofPainting,vol.2,Dover,NewYork,NY,USA,1967.
12. Z.BrochwiczandJ.Rauchfleisz,ApplicationofX-RaySpec-troscopy toIdentificationofInorganicPigments, Library of MuseologyandPreservationofMonuments,vol.34,Warsaw,Poland,1973.
13. P.Rudniewski,Pigments and TheirIdentification,vol. 13, AcademyofFineArts,Warsaw,Poland,1994.
∼1850AD),”
[25]I.M.Bell,R.J.H.Clark,andP.J.Gibbs,“Ramanspectroscopic
library of natural and synthetic pigments (pre-
SpectrochimicaActaA,vol.53,no.12,pp.2159–2179,1997.
[26]A.Nevin,I.Osticioli,D.Anglos,A.Burnstock,S.Cather,andE.
Castellucci, “Raman spectra of proteinaceous materials used in
paintings: a multivariate analytical approach for classificationandidentification,”AnalyticalChemistry,vol.79,no.16,pp.6143–6151,2007.
T.R.Ravindran,A.K.Arora,S.Ramya,R.V.SubbaRao,and
B.Raj,“RamanspectroscopicstudyofmedievalIndianartof17thcentury,”JournalofRamanSpectroscopy,vol.42,no.4,pp.803–807,2011.
1. A.Nevin,D.Comelli,I.Osticiolietal.,“Multi-photonexcita-tion fluorescence and third-harmonic generation microscopy measurements combined with confocal Raman microscopy fortheanalysisoflayeredsamplesofvarnishedoilfilms,”AppliedPhysicsA,vol.100,no.3,pp.599–606,2010.
2. P.Vandenabeele,F.Verpoort,andL.Moens,“Non-destructive analysis of paintings using fourier transform Raman spec- troscopywithfibreoptics,”JournalofRamanSpectroscopy,vol.32,no.4,pp.263–269,2001.

8
Journal of Spectroscopy
[30] K. Castro,
M.
Pe´rez-Alonso,M.D.Rodr´ıguez-Laso,L.A.
Ferna´ndez,andJ.M.Madariaga,“On-lineFT-Ramanand
dispersive Raman spectra database of artists’ materials (e- VISARTdatabase),”AnalyticalandBioanalyticalChemistry,vol.382,pp.248–285,2005.
1. V.S.F.Muralha, L. Burgio, and R.J.H. Clark, “Raman spectroscopy analysis of pigments on 16-17th c.Persianmanuscripts,”SpectrochimicaActaA,vol.92,pp.21–28,2012.
2. A.Deneckere,F.-P.Hocquet,A.Bornetal.,“Directanalysisof the central panel of the so-calledWytstriptych afterJanvanEyck,”JournalofRamanSpectroscopy,vol.41,no.11,pp.1500–1509,2010.
3. J.Zuo,X.Zhao,R.Wu,G.Du,C.Xu,andC.Wang,“AnalysisofthepigmentsonpaintedpotteryfigurinesfromtheHanDynasty’sYanglingTombsby Ramanmicroscopy,”JournalofRamanSpectroscopy,vol.34,no.2,pp.121–125,2003.
4. M. Hanesch, “Raman spectroscopy of iron oxides and(oxy)hydroxides at low laser power and possible applicationsin environmental magneticstudies,”GeophysicalJournalInternational,vol.177,no.3,pp.941–948,2009.
5. C. Pelosi, G. Agresti,U.Santamaria, and E.Mattei,“Artificalyellow pigments: production and characterization throughspectroscopic methods ofanalysis,”E-Preservation Science, vol.7,pp.108–115,2010.
6. R.J.H.Clark,L.Cridland,B.M.Kariuki,K.D.M.Harris,and
R. Withnall, “Synthesis, structural characterisation and RamanspectroscopyoftheinorganicpigmentsleadtinyellowtypesIandIIandleadantimonateyellow:theiridentificationonmedieval paintings andmanuscripts,”Journalof the ChemicalSociety,no.16,pp.2577–2582,1995.
1. I.Borgia,B.G.Brunetti,C.Miliani,C.Ricci,C.Seccaroni,and
  1. Sgamellotti,“Thecombineduseoflead-tinyellowtypeIandIIonacanvaspaintingbyPietroPerugino,”JournalofCulturalHeritage,vol.8,no.1,pp.65–68,2007.
2. C.SandalinasandS.Ruiz-Moreno,“Lead-tin-antimonyyellow: historical manufacture, molecular characterization and iden-tification in seventeenth-century Italianpainting,”StudiesinConservation,vol.49,no.1,pp.41–52,2004.
3. H.G.M.Edwards,D.W.Farwell,E.M.Newton,F.R.Perez,andS.J.Villar,“Ramanspectroscopicstudiesofa13thcentury polychrome statue: identification of a“forgotten” pigment,”JournalofRamanSpectroscopy,vol.31,no.5,pp.407–413,2000.
4. R.J.Meilunas,J.G.Bentsen,andA.Steinberg,“Analysisofaged paint binders by FTIRspectroscopy,”Studies inConservation,vol. 35,pp.33–51,1990.

International Journalof

OrganicChemistryInternational
Hindawi Publishing Corporationhttp://www.hindawi.com
Advances in
PhysicalChemistry
Hindawi Publishing Corporation
International Journal of
MedicinalChemistry
Hindawi Publishing Corporation
International Journal of
AnalyticalChemistry
Hindawi Publishing Corporation
Hindawi Publishing Corporationhttp://www.hindawi.com
http://www.hindawi.com
Volume 2014
Volume 2014
http://www.hindawi.com
Volume 2014
http://www.hindawi.com
Volume 2014
Volume 2014
TheScientific
World Journal
Hindawi Publishing Corporationhttp://www.hindawi.com
Volume 2014

International Journal of
Spectroscopy
Hindawi Publishing Corporation
http://www.hindawi.com	Volume2014

Journal of
Chemistry
Hindawi Publishing Corporation
http://www.hindawi.com	Volume2014

Journal of
Catalysts
Hindawi Publishing Corporation
http://www.hindawi.com	Volume2014

Chromatography ResearchInternational
Hindawi Publishing Corporation
http://www.hindawi.com	Volume2014

Journal of
Theoretical Chemistry
Hindawi Publishing Corporation
http://www.hindawi.com	Volume2014

BioinorganicChemistry andApplications
Hindawi Publishing Corporation
http://www.hindawi.com	Volume2014

Journal of
Applied Chemistry
Hindawi Publishing Corporation
http://www.hindawi.com	Volume2014

International Journal of
Electrochemistry
Hindawi Publishing Corporation
http://www.hindawi.com	Volume2014

International Journal of
Inorganic Chemistry
Hindawi Publishing Corporation
http://www.hindawi.com	Volume2014

Journal of
Spectroscopy
Hindawi Publishing Corporation
http://www.hindawi.com	Volume2014

Journal of
Analytical MethodsinChemistry
Hindawi Publishing Corporation
http://www.hindawi.com	Volume2014

Journal of
Quantum Chemistry
Hindawi Publishing Corporation
http://www.hindawi.com	Volume2014

Submit your manuscripts athttp://www.hindawi.com

International Journal of
Carbohydrate Chemistry
Hindawi Publishing Corporation
http://www.hindawi.com	Volume2014

Photoenergy