Catalysis Today 390-391 (2022) 335-342
Contents lists available at ScienceDirect
Catalysis Today
ELSEVIER
journal homepage: www.elsevier.com/locate/cattod
Platinum nanoparticles supported on zeolite MWW nanosheets prepared via homogeneous solution route
Katarzyna Kałahurskaa , Wojciech Pajerskia , Andrzej Kotarbaa , Martin Kubu h, Yuyan Zhang h,
Michał Mazur h, Jan Prech h, Gabriela Jajkoa , Wacław Makowskia , Wiesław J. Rotha ,
Barbara Gila, ,*
1
"Faculty of Chemi>try, Jagiellonian University in Kraków, Gronostajowa 2, 30-387 Kraków, Poland
1 Department of Physical and Macromolecular Chemi>try, Faculty of Science, Charles University, mavova 8, 12840 Prague 2, Czech Republic
ARTICLE
INFO
ABSTRACT
Keywords:
Pt nanoparticles MWWzeolites Exfoliation
3-nitrotoluene hydrogenation
This article demonstrates preparation of metal functionalized zeolite catalysts via a new homogeneous solution pathway enabled by the recently reported exfoliation of zeolite MWW into solution of unilamellar nanosheets. The preparation is carried out by mixing solutions of exfoliated MWW monolayers and Pt nanoparticles with initial size of ca 3 nm and isolation of such hybrid catalysts by freeze-drying. Optionally, the MWW layer so­ lutions were purified by dialysis prior to mixing with the metal solution, which turned out to be beneficial for quality and textural characteristics. However, catalytic performance in the model reaction - 3-nitrotoluene hydrogenation, was mostly determined by the Pt level, i.e. at least 0.3%, and less affected by the apparent quality of the finał zeolite support. The catalysts revealed agglomeration of the Pt nanoparticles from roughly 3 nm to between 5 and 1O nm.
with controlled dispersion and accessibility via 20-to-30 zeolite trans­ formation for shape-selective catalysis [18] . In generał, 20 zeolites could be manipulated spatially and intercalated with guest molecules and particles larger than their framework pares sizes. The intercalation and layer manipulation processes involve solid-liquid interactions and are also subject to limitations due to charge, layer affinity, reactant solubility and apparently crystal intergrowths. These constrains and the potentia! to design new catalysts have been further expanded by the complete exfoliation into monolayers in solution demonstrated with zeolite MCM-56 with the MWW topology [19] . The exfoliation is carried out as a soft chemical process by reacting MCM-56 with tetrabuty­ lammonium hydroxide (TBAOH) in water that produces zeolite mono­ layers dispersed in a liquid as effectively homogeneous solutions [19]. They allow combination with any additional component 'at will', sub­ ject to compatibility and mutual affinity, which can be also considered adjustable. This work explores the combination of dispersed zeolite layers with Pt nanoparticles as alternatives to the aforementioned 20-to-30 transformation. One of the differences/advantages worth painting to is elimination of the swelling, which requires large excess of surfactant as generally complicated and, if possible, avoidable step.
1. Introduction
Crystalline microporous solids with uniform, nanometer size pares, represented by zeolites, have exceptional value and usefulness in het­ erogeneous catalysis with many large-scale applications in the chemical and petroleum industries [1,2]. As they combine suitable high activity and selectivity with durability, lack of toxicity and ease of production, they are one of the leading catalysts for green chemistry. Zeolites are used by themselves and as supports or active components with other active moieties like metals. The main impediment to the broader application of zeoli tes has been related to their relatively small pore sizes constrained within rigid immutable frameworks. One of the attempted solutions was creation of additional, usually non-uniform, secondary porosity within zeolite structures by soft- or hard-templating, partia! framework elimination, and other methods [3- 8]. A mare controlled approach was presented by the discovery that zeolites can form not only rigid 30 rigid frameworks but also layered 20 structures [9--13] that were amenable to structure modification, espe­ cially expansion [14- 17]. One among many new capabilities enabled by layered zeolites has been the preparation of noble metal nanoparticles
* Correspondence to: Jagiellonian University, Faculty of Chemistry, Gronostajowa 2, 30-387 Kraków, Poland.
E-mail address: barbara.k.gil@uj.edu.pl (B. Gil).
1 0000-0003-4096-0762.
https://doi.org/10.1016/j.cattod.2021.09.026
Received 28 June 2021; Received in revised form 4 September 2021; Accepted 23 September 2021
Available online 25 September 2021
0920-5861/© 2021 The Authors. Published by Elsevier B.V. This is an open access article under the CC BY license (htt p:/ / creativecommons.org/ licenses/b y/ 4.0/ ).

K. Kalahurska et al.
Catalysi> Today 390-391 (2022) 335-342
Metal nanoparticles (NPs) are of great interest for catalysis and have been extensively studied [20- 27]. Nanoclusters and subnanoclusters of platinum (< 1 nm) have shown superb catalytic properties, which result from the small particie size and thus, high dispersion of active compo­ nents [28] . Decreasing size of metal nanoparticle usually results in higher and faster conversion of substrates, but as shown by Guo et al. [29], there is typically an optimum size for best performance. Addi­ tionally, there is a tendency for irreversible aggregation of nanoparticle clusters resulting in a considerable recent effort to prevent that [30,31]. Dispersing metal particles on solid supports remains the most effective way to alleviate metal aggregation. Much attention was already given to promising solid supports, such as graphite [32], polymers [33 ], metal oxides [34] and zeolites [35-3 8].
The model reaction used in this study is hydrogenation of 3-nitroto­ luene. Transformation of nitroarenes to anilines is of great practical importance owing to the usage of resulting anilines for dyestuffs and pharmaceuticals [39,40]. Furthermore, catalytic hydrogenation using high-pressure hydrogen with supported Pt as a catalyst is the preferred process [41 ]. Various support materials prepared by different methods exhibit substantial differences in catalytic activity. Zeolite based Pt-MWW materials can compete with different systems by showing fast conversion and high selectivity to m-toluidine as the only product [18]. The solutions ofzeolite monolayers that are currently available with the MWW topology but are possible with other frameworks, can be combined with prepared metal nanoparticles in a second solution and eventually isolated as intimately mixed solids/catalysts. Such processes have many parameters that need investigation for optimized perfor­ mance and benefits, e.g. synthesis and cost, that are very likely to depend on a particular catalytic reaction. Herein, we demonstrate high catalytic activity of the catalysts prepared from exfoliated monolayers and Pt nanoparticles and examine the effects of same basie properties
and treatments during preparation.
with Pt-nanoparticle solutions described below. Typical pH was 12.
2.3. Dialysis of the MWW nanosheet solutions
The dialysis was carried out as an optional purification/pH reduction step. Supernatant solutions with MWW layers were poured into a dial­ ysis tubing cellulose membrane with the cutoff of 14,000 Daltons (Sigma-Aldrich) and immersed in excess deionized water. The external solvent was stirred and changed repeatedly, until the desired pH was obtained.
2.4. Synthesis of the platinum nanoparticles
Citrate-capped platinum nanoparticles were synthesized with the protocol described elsewhere [43]. In a typical procedure, 2 ml of H2PtC16 (16.0 mM) and 2 ml ofTSC (40.0 mM) were added to 76 ml of deionized water and stirred for 30 min at room temperature. Next, 200 µl of NaB H4 (50.0 mM) was added dropwise and the reaction mixture was stirred vigorously for 1 h at ambient temperature. The typical particie size was 1.5-3.5 nm.
2.5. Preparation of MWW zeolite-Pt samples
Solutions with platinum nanoparticles were added dropwise to 40 ml of the solutions of MWW nanosheets with stirring. The mixture was stirred for additional 20 min and lyophilized. The following solution ratios were used to obtain desired Pt contents: 1:1.175 (0.8% Pt w/w), 1:0.44 (0.3% Pt w/w), and 1:0.30 (0.2% Pt w/w).
2.6. Freeze-drying
The solutions of Pt nanoparticles and MWW monolayers (50-90 ml) were frozen for 30 min in a shell bath freezer to - 42 °c, with integrated rotate system and then attached to the lyophilizer (Labconco®) and maintained under vacuum (0.1 mbar) for overnight, affording low density powder.
2. Materials and methods
All reagents used in the experiments were purchased from Sigma­ Aldrich except trimethylacetonitrile (Avantor Performance Materials Poland), trisodium citrate dihydrate (TSC, Avantor Performance Mate­ rials Poland), ammonium nitrate (NH4NO3, Avantor Performance Ma­
2.7. Sample preparation for catalysis
terials Poland), sodium aluminate Riedel-de- Haen).
(40-45%
Na2O,
50-56% AbO3,
The obtained Pt-MWW zeolite samples were calcined at 540 °C for 6 h to remove the template and other organie residue, and ion exchanged into the NH4+ form, by stirring with 1 M solution of NH4NO3 for 1 hat room temperature (20 ml of NH4NO3 per 0.5 g zeolite). The exchange was carried out three times, then samples were filtered, washed with deionized water and dried at room temperature.
2.1. Synthesis of MCM-56
MCM-56 was prepared by the published procedure [19,42] . The synthesis mixture comprised the following reagents: silica (nanopowder with particie size 10-20 nm), 50% NaOH solution, sodium aluminate, 98% hexamethyleneimine (HMI) and deionized water combined with the molar ratios: 1 SiO2: 0.04 Al2O3: 0.093 Na2O: 0.3 HMI: 16 H2O. The
hydrothermal synthesis was carried out in a sealed Teflon-lined auto­
clave with rotation, initially by aging for 12 hat room temperature, and then with heating at 145 °C for 38 h. The solid product was isolated by filtration, washed with deionized water and dried at room temperature. Its quality was verified by powder X-ray diffraction (XRD) and textural parameters.
2.8. Catalyst characterization
Fourier-Transform Infrared Spectroscopy (FT-IR) was used to deter­ mine the concentration of Bnosnsted (BAS), Lewis (LAS) and external Bn,msted (BASext) sites. Pyridine (kinetic diameter 0.54 nm [44]) adsorption allowed to determine BAS and LAS concentration, using in­
tensity of the 1545 cm- 1 band of protonated pyridine, and the 1450 cm- 1 band of coordinatively bonded pyridine with respective absorp­
tion coefficients: s(BAS) = 0.044 cm2/ µmol, s(LAS) = 0.165 cm2/ µmol
[45]. Trimethylacetonitrile (pivalonitrile, kinetic diameter 0.62 nm [44]) interacts only with Bnosnsted acid sites at the external surfaces and pore mouths. External Bn,msted acid sites (BASext) concentration was estimated by integration of the 3620 cm- 1 maximum, characteristic of Si-OH-Al group, i.e. BAS [ 46] measured before and after trimethylace­ tonitrile adsorption. Self-supporting pellets of mass between 15 and 20 mg were prepared from zeolite powders, and transferred to a home-made FT-IR cell, allowing activation and adsorption inside FT-IR spectrometer. Samples were calcined at 490 °C for 1 h under vacuum (- 10-5 mbar). Before the adsorption of probe molecules the system was cooled to the proper adsorption temperature: 170 °C for pyridine,
2.2. Exfoliation and purification of MWW monolayer solutions
The published two-step procedure was followed [19] . 0.5 g of MCM-56 was stirred for 1.5 h with 27 g of 11 % tetrabutylammonium hydroxide (TBAOH) solution and centrifuged for 20 min at 10,000 rpm in a 50 ml fakon tube (Karteli, non-sterile). The supernatant was dec­ anted and discarded. 40 ml of water was added to the wet sediment, stirred for 1.5 h and centrifuged like before. The obtained translucent supernatant solution containing unilamellar MWW nanosheets [19], was carefully decanted and used, as-is or after dialysis, for combination
336

K. Kalahurska et al.
Catalysi> Today 390-391 (2022) 335-342
+11.5% TBAOH
stirring, centrifugation, decantation
+water
stirring, centrifugation
MWW rnonolayers
in solution
+Pt nanoparticles
Scheme 1. Preparation steps leading to Pt-MWW materials.
ambient temperature for pivalonitrile. After adsorption of the vapors (at ca. 20 mbar equilibrium pressure) the gas phase together with weakly adsorbed species were evacuated at the adsorption temperature for 20 min. FT-IR measurements were carried out using the Bruker Tensor 27 spectrometer equipped with an MCT detector having the spectra! reso­ lution of2 cm- 1.
The solid products were characterized by X-ray diffraction (XRD) using Rigaku MiniF!ex diffractometer in refection made, CuKa radiation (A= 0.154 nm) in the ranges 28 = 3-35°. The XRD patterns were usually collected with steps of 0.02°.
Adsorption/desorption isotherms of nitrogen at - 196 °C were determined using static volumetric Autosorb IQ apparatus (Quantach­ rome Instruments). All samples were activated under vacuum for 1 h at 80 °c, 1 hat 120 °C and 8 hat 350 °C (2 °C/min). Specific surface area values were determined using the BET method, based on the recom­ mendation concerning characterization of microporous materials [47]. Thet-plot method was used to determine the external surface area and micropore volume values.
TEM measurements were performed using an FEI SITEM Titan in­ strument operating at an accelerating voltage of 300 kV. TEM visuali­ zation was also carried out using JEOL NeoARM 200 F operating at 200 kV. STEM images were collected using annular dark field detector. Powder samples were deposited on the EMR Holey Carbon support film on copper 300 square mesh. Microscope was aligned by the standard method using sample covered with gołd nanoparticles. The measure­ ments were carried out to assess the morphology and size distribution of the synthesized platinum nanoparticles. TEM images were analyzed
using the Java open-source ImageJ 1.51k software [48].
2.9. Catalytic testing
The model catalytic reaction was performed in PIO 4 Parallel Stirred Tanks Ppcstrl 9003. Before the reaction, the Pt-MWW catalysts were reduced in a tube oven with 150 ml/min H2/ N2 (v:v = 1:1) at 500 °C for
5 h (4 °C/min). Catalytic reactors with 50 ml volume were loaded with
- 7.5 mmol of 3-nitrotoluene (Sigma Aldrich, 99%), - 50 mg catalysts (Pt-MWW or Pt/ Al20 3 - Sigma Aldrich, 1% loading), - 2.5 mmol n­ dodecane (Sigma Aldrich, 98%, interna! standard), and 30 ml n-hexane (VWR Chemicals, 100%). After reaching 100 °c, the autoclave was
pressurized with 6 bar H2 and stirring was fixed at 800 rpm. Samples of the reaction mixture were withdrawn after O, 15 min, 30 min, 1 h, 2 h, 4 h, and 6 h of the reaction. The sampies were centrifuged to remove the catalyst and analyzed by gas chromatography using a gas chromato­ graph Agilent 7890B GC equipped with HP-5 column (length 30 m, diameter 0.32 mm, and film thickness 0.25 µm).
The conversion of 3-nitrotoluene (Conv.) and was calculated ac­ carding to Eq. (1) :
N 3n feed- N 3n pr
Conv(%)
•100%
(1)
N3n feed
where N3n feed is the amount of 3-nitrotoluene (moles) in the feed; N3n pr is the amount of 3-nitrotoluene (moles) in the products mixture. All N values used in Eq. (1) were calculated based on the interna! standard
calibration method, using n-dodecane as an interna! standard and
337

0.8Pt-MWW-dl

0.2Pt-MWW-dl

+Pt nanoparticles

dialysis

0.3Pt-MWW

MWW rnonolayers in solution

MWW
MCM-56 as synthesized

K. Kalahurska et al.
Catalysi> Today 390-391 (2022) 335-342
ways, especially by size and charge as obstacles to mutual component penetration and intimate mixing. These impediments are in principle absent and the synthesis is readily implemented in the systems presented herein, because they are based on forming homogeneous liquid solu­ tions. One of the important parameters that may be critical for activity and cost, is the relative amount the metal, so it was investigated as the primary variable, between nominał 0.2--D.8% Pt metal. The preparations proved to be straightforward and produced the desired outcome of Pt-nanoparticles with representative sizes below 10 nm well dispersed within the zeolite matrix. This was confirmed by TEM and mare detailed physical characterization. Most notably, the obtained catalysts showed potentia! for high activity, dependent on Pt level, in a model reaction - 3-nitrotoluene hydrogenation, with performances comparable to a commercial catalyst. The preparation and differences between the pro­ duced catalysts are shown in Scheme 1. The adopted sample designation includes %Pt and optional -dl at the end (as dialysis if applied, e.g. 0.2Pt-MWW-dl).
In all preparations the original framework was preserved but there was same variation in basie zeolite characteristics: XRD, textural prop­ erties and acidity, which turned out to be less crucial for high catalytic activity.
Powder X-ray diffraction patterns of the Pt-nanoparticle-MWW layers (Pt-MWW) after calcination, shown in Fig. 1, contain the finger­ print reflections at ca. 7.1°, 14.2°, 25° and 26°28 (CuKa radiation; d­
spacing: 1.25, 0.625, 0.356, 0.342 nm) confirming the MWW structure
[50]. The original MCM-56 samples show the characteristic broadband between 8° and 10°28, assigned to disorganized MWW layers but with a slight dip, interpreted as partia! ordering due to calcination [51]. In the Pt-MWW this band is not well defined because there is an additional distinct broad maximum arising near 10°28. The latter was already re­ ported in our previous publication concerning MWW layers isolated after exfoliation [52] but its origin and assignment are obscure. One of the possibilities may be that it is related to the 003 reflection. The
::i
4000
ro
i.:;;
C
C
2000
5	10	15	20	25	30	35
20, deg.
Fig. 1. XRD
patterns of MCM-56 with platinum nanoparticles
and their
parent (MWW).
commercially available 3-nitrotoluene. For identification of the product m-toluidine (Sigma Aldrich, 99%) was used.
3. Results and discussion
The primary goal of this work has been the preparation and valida­ tion of a new type of zeolite-metal nanoparticle catalysts that have been enabled by the availability of exfoliated zeolite monolayer solutions. The liquid dispersions of zeolite monolayers and metal nanoparticles in solutions are prepared separately and combined into homogeneous so­ lutions from which intimate solid mixtures can be isolated. Freeze­ drying was the chosen method of isolation as it ensured full recovery of all components. Before the reported exfoliated zeolite layers in so­ lution [19] become available the only possible synthetic pathways were based on solid-liquid treatments [44,49], which are constrained in many
60
0.2Pt-MWW-dl
Pt nanoparticles
60
'?fi!.
u>
C:
QJ
:::,
40
40
...
O"
QJ
20
u..
20
o
o
o
o
5
10 15 20 25
30 35
5
10 15 20 25
30
35
30
0.8Pt-MWW-dl
0.3Pt-MWW
60
'?fi!.
u>
C:
QJ
:::,
20
40
...
O"
QJ
10
u..
20
o
o
o
o
5
10 15 20 25
particie size, nm
30
35
5	10 15 20 25
particie size, nm
30 35
Fig. 2. Particie size distribution (PSD) in the original platinum nanoparticles solution, in calcined and ammonium exchanged Pt-MWW materials (darker colors) and after reduction with H2 (striped).
338

K. Kalahurska et al.
Catalysi> Today 390-391 (2022) 335-342
0.2Pt-MWW-dl
0.3Pt-MWW
0.8Pt-MWW-dl
.
0.2Pt-MWW-dl
0.3Pt-MWW
0.8Pt-MWW-dl
•
..
• •
•
•
•
0.2Pt-M WW -dl
0.8Pt-M WW-dl
MWW, SAED
Fig. 3. Selected TEM images for the Pt-MWW materials (rows 1 and 2), close-up view of selected samples of the Pt nanoparticles (bottom left) and SAED of the zeolite (bottom right).
Table 1
Acid sites concentration based on the sorption of pyridine (tata! Brpnsted and Lewis acid sites, BAS and LAS) and pivalonitrile (external Brpnsted acid sites, BASext) determined by FT-IR spectroscopy, and textural properties calculated from nitrogen adsorption isotherms (specific surface area BET, micropore volume, and external surface area).
Surface area, m2/ g
Pore volume, cm3/g
Acid sites concentration, µmol/g
Sample
BAS
1028
826
554
831
LAS
BASext

376
196
254
253
Vmicro
0.104
0.092
o
0.070
SBET
Sext
MWW
0.2Pt-MWW-dl
0.3Pt-MWW
0.8Pt-MWW-dl
504
507
255
431
201
291
329
269
142
158
98
141
339

•

. .	•.,...	.
..	•	..
f

.•	•
•
•.. .

Catalysi, Today 390-391 (2022) 335--342
K. Kalahurska et al.
--MWW
600
600
""6
zN
""e 400
400
u
zN
VI
VI
"'C
ro 200
200
O-+-
-
0.6
- _,
0.8	1.0
O+-
-
0.4
-
--ł
o.o	0.2
o.o	0.2
0.4
0.6
0.8
1.0
p/po
p/po
Fig. 4. N2 adsorption isotherms for parent MWW and Pt-MWW sampl es.
Pt-MWW materials show amplified low angle reflections at 3.8°20, which are not the 001 reflections but due to 11011-Bragg diffraction caused by thin crystal dimension along the z axis [53,54] . The observed intensity amplification may indicate that due to Pt-nanoparticles the layers reveal mare unilamellar character that when they condense without intervening particles. The sample obtained without dialysis of the solution with MWW layers has visibly !ower crystallinity, which is also reflected in lowered textural parameters. Evidently, dialysis is conducive to higher crystallinity and porosity, but these parameters are not crucial for the eventual overall catalytic performance.
Particie size distributions of the Pt nanoparticles are showu in Fig. 2. The original nanoparticles in solution are not larger than 3.5-4 nm. The dominant size fractions are 2.5 nm (62%) and 1.5 nm (30%). The size of Pt nanoparticles in the zeolite matrix after cakination is increased to between 5 and 10 nm for the most abundant fraction and the size dis­ tribution is broadened. There is evident agglomeration and the resultant particles have continuous crystalline structure . Larger amount of Pt, namely 0.8%, leads to bigger particles overall, so the smaller amounts, like 0.3% seem optima! (for cost reasons too) (Fig. 3).
The combined results of textural properties calculated from nitrogen adsorption isotherm (specific surface area BET, micropore volume, and external surface area) and concentration of Bn <Snsted active sites are summarized in Table 1.
For the Pt-MWW samples the finał textural properties are greatly influenced by pre-purification of the MWW nanosheet solutions by dialysis: the dialyzed ones, 0.2% and 0.8% Pt, showed significant micropore volume and BET surface areas, comparable to the source MCM-56 materials . In contrast, the undialyzed MWW solution resulted in the end in depressed textural properties and also lowered apparent crystallinity (0.3%Pt). The dialyzed Pt-MWW samples showed ca. 300/4 higher external surface area and ca. 50% higher Bnmsted acidity with respect to the sample not subjected to dialysis. The observed differences, especially the apparent !ower quality of the undialyzed sample were not critical for catalytic performance.
There is a visible qualitative change in the isotherms (Fig. 4) between the original MCM-56 and the Pt-MWW products. The farmer show large vertical hysteresis above p/ p0 > 0.8, attributable to relatively large interparticle voids - it is type H2b due to pore blocking/percolation in a wide range of pore openings [47] . The dialyzed Pt-MWW samples showed very similar adsorption isotherms with a H3/ H4 horizontal hysteresis loops, often exhibited by 11011-rigid a gglomerate s, platy-shaped microporous materials (H3) or aggregates of zeolite crys­
tals (H4) [47]. The isotherm observed for the undialyzed sample is shifted down, which indicates significantly !ower microporosity, and exhibits slightly larger slope indicating larger external surface. The fact that the BET surface is !ower than the external surface areas is surprising
80
'#.
60
c.'
o
".i.i.i
a,
40
o
u
-+-
-+-
-+-
-+-
commercial 0.8Pt-M WW-dl
0.3Pt-M WW
0.2Pt-MWW-dl
20
o
100
200
time, min
300
400
Fig. 5. Catalytic test resul ts of 3-nit rotoluene hydrogenation .
but not erroneous, because both values were calculated using different formalism based on different geometrical models, therefore they have limited physical meaning and are not commensurate. 0.3Pt-MWW sample shows discrepancy between the data from nitrogen adsorption measurements (in which this materia! appears as 11011-porous) and acidity and catalysis data (which indicate considerable content of accessible acid sites, typical for zeolitic frameworks). A possible expla­ nation of this effect is blocking the micropores by Pt nanoparticles, effective at liquid nitrogen temperature and ineffective at higher tem­ peratures (due to thermal expansion and framework dynamics).
External acidity of all Pt-doped sampies was significantly !ower with respect to the source materials. BAS concentra tion decreased by ca. 25% (ca. 200 µmo!/g) for the dialyzed samples and this loss is mainly due to the decrease of the BASexr co ncentra tion, which diminished from 376 to 200-250 µmo!/g even as the external surface area increased . This can be accounted for, since Pt nanoparticles are located in the interparticle region, and their presence does not influence the interna! (intralayer) acidity. At the same time pyridine was able to react with all BAS present, since the intensity of the Si-OH-Al maximum after pyridine adsorption disappeared (spectra not showu), which indicated that interior of the
340
._	0.8Pt-MWW-dl
._	0.3Pt-MWW
._	0.2Pt-MWW-dl

K. Kalahurska et al.
Catalysi> Today 390-391 (2022) 335-342
layers was not blocked by the deposited nanoparticles. Much higher decrease of BAS concentration (ca. 50%) together with negligible micropore volume shown by the undialyzed sample highlights the importance of additional purification but is hard to explain in detail. On the other hand, such purification, e.g. by dialysis, was not crucial for hydrogenation activity as already emphasized above. This indicates the importance of colloid purification, in our case made by dialysis, in processes in which acidity is equally important as activity provided by nanoparticles.
As the finał and most consequential evaluation, the obtained Pt­ MWW materials were tested in a model catalytic reaction of 3-nitroto­ luene hydrogenation (Fig. 5). The top conversion was comparable to a commercial catalyst, validating the generał synthetic methodology and approach to producing competitive catalyst. The three studied samples showed differences in activity (with 100% selectivity to 3-aminoto­ luene), which are difficult to correlate with determined physical char­ acteristics and acidity but point to a rationale that there is a minimum level for Pt, 0.3%, to achieve maximum conversion and above that the performance levels off. The 0.2% Pt catalyst is visibly less active than those 0.3% Pt and up. As already emphasized the nominał quality based on XRD, textural properties and acidity are less critical. In the same vain, dialysis affords better quality materials based on these properties but does not affect catalytic performance at this level. Possible sintering of Pt nanoparticles during activation of the catalysts in hydrogen at high temperature was ruled out on the basis of particie size distribution by TEM imaging. The overall distribution of the particie sizes was not changed considerably as shown in Fig. 2 (corresponding images of the H2-treated catalysts are presented in Fig. Sł , Supplementary materia ]).
interests or personal relationships that could have appeared to influence the work reported in this paper.
Acknowledgments
This work was financed with the funds from the National Science Centre, Poland, Grant no. 2020/37/B/ST5/01258 (WJR and BG). KK has been partly supported by the National Centre for Research and Devel­ opment, Poland, EU Project POWR.03.02.00-00-I004/16. MK and YZ acknowledge the support of the Czech Science Foundation, Czech Re­ public, to the project EXPRO (19-27551X).
Glassware for graphical abstract designed by macrovector/brgfx/ Freepik.
Appendix A. Supplementary materiał
Supplementary data associated with this article can be found in the online version at doi:10.1016/ j.cattod.2021.09.026 .
References
A.F. Masters, T. Maschmeyer, Zeolites - from curiosity to cornerstone, Microporous
Mesoporous Mater. 142 (2011) 423- 438.
I. Fechete, Y. Wang, J.C. Vedrine, The past, present and future of heterogeneous catalysis, Catal. Today 189 (2012) 2- 27.
D. Verboekend, S. Mitchell, J. Perez-Ramirez, Hierarchical zeolites overcome all
obstacles: next stop industrial implementation, Chimia 67 (2013) 327- 332.
D. Verboekend, J. Perez-Ramirez, Design of hierarchical zeolite catalysts by desilication, Catal. Sci. Techno!. 1 (2011) 879-890 .
D. Verboekend, R. Caicedo-Realpe, A. Bonilla, M. Santiago, J. Perez-Ramirez, Properties and functions of hierarchical ferrierite zeolites obtained by sequential post-synthesis treatments, Chem. Mater. 22 (2010) 4679- 4689 .
[1]
[2]
[3]
[4]
[5]
4. Conclusions
[6] J. Perez-Ramirez, D. Verboekend, A. Bonilla, S. Abello, Zeolite catalysts with
tunable hierarchy factor by pore-growth moderators, Adv. Funct. Mater. 19 (2009)
3972- 3979 .
[7] J. Perez-Ramirez, C.H. Christensen, K. Egeblad, C.H. Christensen, J.C. Groen, Hierarchical zeolites: enhanced utilisation of microporous crystals in catalysis by advances in rnaterials design, Chern. Soc. Rev. 37 (2008) 2530- 2542.
Zeolite MWW monolayers, 2.5 nm thick, exfoliated into solution were combined with solution of Pt nanoparticles, and isolated as inti­ mately mixed solid catalysts. This represents an unprecedented approach to preparation of bifunctional catalysts, which to date was carried out exclusively via heterogeneous solid-liquid interactions. 3 different levels of platinum incorporation were targeted: 0.2%, 0.3% and 0.8% w/w with optional purification of the MWW solutions by dialysis after exfoliation. The obtained catalysts were tested in a model nitrotoluene hydrogenation and those with Pt content above 0.2% showed activity comparable to a benchmark commercial catalyst. Physical characterization showed that the applied dialysis was benefi­ cial for XRD quality and textural properties but did not matter much for catalytic activity, which depended mostly on the amount of Pt, specif­ ically to be at sufficiently high level (0.3% in this case). The finał cat­ alysts showed moderate increase in size of the Pt nanoparticles from ca. 3 nm to between 5 and 10 nm for the most represented size fraction. The demonstrated approach can be extended to both other exfoliated layered zeolites as they become available and other nanoparticles relevant for catalysis. The synthesis itself has many variables for optimization that may vary depending on a particular process.
[8]
J.C. Groen, J.A. Moulijn, J. Perez-Ramirez, Decoupling mesoporosity formation and acidity modification in ZSM-5 zeolites by sequential desilication ­ dealumination, Microporous Mesoporous Mater. 87 (2005) 153-161.
L. Xu, P. Wu, Diversity of layered zeolites: from synthesis to structural modifications, New J. Chern. 40 (2016) 3968--3981.
[9]
[10] W.J. Roth, B. Gil, B. Marszałek, Comprehensive system integrating 3D and 2D
zeolite structures with recent new types of layered geometries, Catal. Today 227
(2014) 9-14 .
U. Diaz, A. Corma, Layered zeolitic materials: an approach to designing versatile
functional solids, Dalton Trans. 43 (2014) 10292- 10316 .
1. W.J. Roth, D.L. Dorset, Expanded view of zeolite structures and their variability based on layered nature of 3 -D frameworks, Microporous Mesoporous Mater. 142 (2011) 32-36 .
2. M. Choi, K. Na, J. Kim, Y. Sakarnoto, O. Terasaki, R. Ryoo, Stable single-unit-cell nanosheets of zeolite MF! as active and long-lived catalysts, Nature 461 (2009) 246- 249.
3. L. Wei, K.C. Song, W. Wu, S. Holdren, G.H. Zhu, E. Shulman, W.J. Shang, H.
Y. Chen, M.R. Zachariah, D.X. Liu, Vapor-phase strategy to pillaring of two­ dimensional zeolite, J. Am. Chem. Soc. 141 (2019) 8712- 8716.
W.J. Roth, B. Gil, A. Mayoral, J. Grzybek, A. Korzeniowska, M. Kubu,
W. Makowski, J. Cejka, Z. Olejniczak, M. Mazur, Pillaring oflayered zeolite precursors with ferrierite topology leading to unusual molecular sieves on the micro/mesoporous border, Dalton Trans. 47 (2018) 3029- 3037.
H. Gies, U. Muller, B. Yilmaz, T. Tatsumi, B. Xie, F.S. Xiao, X.H. Bao, W.P. Zhang,
D. De Vos, Interlayer expansion of the layered zeolite precursor RUB-39: a universal method to synthesize functionalized microporous silicates, Chem. Mater. 23 (2011) 2545- 2554.
1. W.J. Roth, C.T. Kresge, J.C. Vartuli, M.E. Leonowicz, A.S. Fung, S.B. McCullen, MCM-36: the first pillared molecular sieve with zeolite properties, Catal. Microporous Mater. 94 (1995) 301- 308.
2. Y. Zhang, K. Fulajtarova, M. Kubu, M. Mazur, M. Shamzhy, M. Hronec, J. Cejka, Controlling dispersion and accessibility of Pd nanoparticles via 2D-to-3D zeolite transformation for shape-selective catalysis: Pd@MWW case, Mater. Today Nano 8 (2019), 100056.
3. W.J. Roth, T. Sasaki, K. Wolski, Y. Song, D.M. Tang, Y. Ebina, R.Z. Ma, J. Grzybek,
K. Kalahurska, B. Gil, M. Mazur, S. Zapotoczny, J. Cejka, Liquid dispersions of zeolite monolayers with high catalytic activity prepared by soft-chemic al exfoliation, Sci. Adv. 6 (2020) 8163.
K. Arnent, D.R. Wagner, T. Gotsch, T. Kikuchi, J. Krohnert, A. Trunschke,
T. Lunkenbein, T. Sasaki, J. Breu, Enhancing the catalytic activity of palladium nanoparticles via sandwich-like confinement by thin titanate nanosheets, Acs Catal. 11 (2021) 2754- 2762.
CRediT authorship contribution statement
Katarzyna Kałahurska: Investigation, Conceptualization, Writing - original draft. Wojciech Pajerski: Investigation. Andrzej Kotarba: Investigation. Martin Kubu: Investigation. Yuyan Zhang: Investiga­ tion. Michał Mazur: Investigation. Jan Prech: Investigation. Gabriela Jajko: Investigation. Wacław Makowski: Writing - review & editing. Wiesław J. Roth: Conceptualization, Funding acquisition, Writing - original draft, Writing - review & editing. Barbara Gil: Investigation, Writing - original draft, Writing - review & editing.
Declaration of Competing Interest
The authors declare that they have no known competing financial
341

K. Kalahurska et al.
Catalysi> Today 390-391 (2022) 335-342
[21]
D. Astruc, Introduction: nanoparticles in catalysis, Chem. Rev. 120 (2020) 461- 463.
J.Y. Cheon, S.J. Kim, W.H. Park, Facile interpretation of catalytic reaction between
organie dye pollutants and silver nanoparticles with different shapes,
J. Nanomater. 2019 (2019) 1-8 .
E.K. Dann, E.K. Gibson, R.H. Blackmore, C.R.A. Catlow, P. Collier, A. Chutia, T.
E. Erden, C. Hardacre, A. Kroner, M. Nachtegaal, A. Raj, S.M. Rogers, S.F.R. Taylor,
P. Thompson, G.F. Tierney, C.D. Zein alipo ur-Yazdi, A. Goguet, P.P. Wells, Structural selectivity of supported Pd nanoparticles for catalytic NH 3 oxidation resolved using combined operando spectroscopy, Nat. Catal. 2 (2019) 157-163 .
R. Grisel, K.J. Weststrate, A. Gluhoi, B.E. Nieuwenhuys, Catalysis by gołd nanoparticles, Gold Bull. 35 (2002) 39- 45.
1. S. Goel, Z. Wu, S.I. Zones, E. Iglesia, Synthesis and catalytic properties of metal clusters encapsulated within small-pore (SOD, GIS, ANA) zeolites, J. Arn. Chem. Soc. 134 (2012) 17688- 17695.
2. I. Sorribes, A. Corma, Nanolayered cobalt- molybdenum sulphides (Co-Mo-S) catalyse borrowing hydrogen G-S bond formation reactions of thiols or H2S with alcohols„ Chem. Sci. 10 (2019) 3130- 3142.
3. J. Song, Z.-F. Huang, L. Pan, K. Li, X. Zhang, L. Wang, J.-J. Zou, Review on selective hydrogenation of nitroarene by catalytic, photocatalytic and electrocatalytic reactions, Appl. Catal. B: Environ. 227 (2018) 386- 408.
4. A.-M. Alexander, J.S.J. Hargreaves, Alternative catalytic materials: carbides,
nitrides, phosphides and amorphous boran alloys, Chem. Soc. Rev. 39 (201O) 4388-4401.
1. W.J. Roth, P. Chlubna, M. Kubu, D. Vitvarova, Swelling of MCM-56 and MCM-22P with a new mediu m - surfactant-tetra methylammoniu m hydroxide mixtures, Catal. Today 204 (2013) 8-14 .
2. G.W. Wu, S.B. He, H.P. Peng, H.H. Deng, A.L. Liu, X.H. Lin, X.H. Xia, W. Chen,
Citrate-capped platinum nanoparticle as a smart probe for ultrasensitive mercury
sensing, Ana!. Chem. 86 (2014) 10955-10960 .
E. Schulman, W. Wu, D. Liu, Two-dimension al zeolite materials: structural and
acidity properties, Materials 13 (2020) 1822.
B. Gil, W.J. Roth, W. Makowski, B. Marszałek, D. Majda, Z. Olejniczak,
P. Michorczyk, Facile evaluation of the c1ystallization and quality of the transient layered zeolite MCM-56 by infrared spectroscopy, Catal. Today 243 (2015) 39- 45.
1. B. Gil, K. Kalalmrska, A. Kowalczyk, A study of the external and interna! sites of 2D and 3D zeolites through the FTIR investigation of the adsorption of arnmonia and pivalonitrile, Appl. Catal. A: Gen. 578 (2019) 63- 69.
2. M. Thommes, K. Kaneko, A.V. Neimark, J.P. Olivier, F. Rodriguez-Rei noso,
J. Rouquerol, KS.W. Sing, Physisorption of gases, with special reference to the evaluation of surface area and pore size distribution (IUPAC technical report), Pure Appl. Chem. 87 (2015) 1051- 1069.
1. C.A. Schneider, W.S. Rasband, K.W. Eliceiri, NIH image to ImageJ: 25 years of image analysis, Nat. Methods 9 (2012) 671- 675.
2. W.J. Roth, B. Gil, W. Makowski, B. Marszałek, P. Eliasova, Layer like pornus materials with hierarchical structure, Chem. Soc. Rev. 45 (2016) 3400- 3438 .
3. W.J. Roth, D.L. Dorset, G.J. Kennedy, Discove1y of new MWW farnily zeolite EMM- 10: identification of EMM-l 0P as the missing MWW precursor with disordered layers, Microporous Mesoporous Mater. 142 (2011) 168- 177.
4. W.J. Roth, J. Cejka, R. Millini, E. Montanari, B. Gil, M. Kubu, Swelling and interlayer chemistry of layered MWW zeolites MCM-22 and MCM-56 with high Al content, Chern. Mater. 27 (2015) 4620- 4629.
5. K. Kalahurska, P.P. Ziemianski, W.J. Roth, B. Gil, Prom colloidal dispersions of zeolite monolayers to effective solid catalysts in transformations of bulky organie molecules: role of freeze-drying and dialysis, Molecules 26 (2021), 2076.
6. G.G. Juttu, R.F. Lobo, Characterization and catalytic properties of MCM-56 and MCM-22 zeolites, Microporous Mesoporous Mater. 40 (2000) 9- 23.
7. J.L. Schlenker, B.K. Peterson, Computed X-ray powder diffraction patterns for ultrasmall zeolite crystals, J. Appl. Crystallogr. 29 (1996) 178- 185.
[22]
[23]
[24]
[25] S.C. Kim, W.G. Shim, M.S. Lee, S.C. Jung, Y.K. Park, Preparation of platinum nanoparticle and its catalytic activity for toluene o:xidation, J. Nanosci. Nanotechnol. 11 (2011) 7347- 7352.
[26]
R.M. Rioux, H. Song, M. Grass, S. Habas, K. Niesz, J.D. Hoefelmeyer, P. Yang, G.
A. Somorjai, Monodisperse platinum nanoparticles of well-defined shape: synthesise characterization, catalytic properties and future prospects, Top. Catal. 39 (2006) 167- 174.
E. Shahbazali, V. Hesse!, T. Noel, Q. Wang, Metallic nanoparticles made in flow and their catalytic applications in organie synthesis, Nanotechnol. Rev. 3 (2014) 65- 86.
T. Imaoka, H. Kitazawa, W.J. Chun, K. Yamamoto, Finding the most catalytically active platinum clusters with low atomicity, Angew. Chem. Int. Ed. 54 (2015) 9809- 9815.
K. Guo, H. Li, Z. Yu, Size-dependent catalytic activity of monodispersed nickel nanoparticles for the hydrolytic dehydrogenation of ammonia borane, ACS Appl. Mater. Interfaces 10 (2018) 517- 525.
[27]
[28]
[29]
1. S.L. Allen, J.N. Sharma, F.P. Zamborini, Aggregation-dependent oxidation of metal nanoparticles, J. Am. Chem. Soc. 139 (2017) 12895- 12898 .
2. B. Gilbert, R.K. Ono, KA. Ching, C.S. Kim, The effects of nanoparticle aggregation processes on aggregate structure and metal uptake, J. Colloid Interface Sci. 339 (2009) 285- 295.
3. B. Bowden, M. Davies, P.R. Davies, S. Guan, D.J. Morgan, V. Roberts, D. Wotton, The deposition of metal nanoparticles on carbon surfaces: the role of specific functional groups, Faraday Discuss. 208 (2018) 455- 470.
4. G. Romanazzi, A.M. Fiore, M. Mali, A. Rizzuti, C. Leonelli, A. Nacci, P. Mastrorilli,
M.M. Dell' Anna, Polymer supported Nickel nanoparticles as recyclable catalyst for
the reduction of nitroarenes to anilines in aqueous medium, Mol. Catal. 446 (2018) 31- 38.
1. C.H. Mejia, J.E.S. van Der Hoeven, P.E. de Jongh, K.P. de Jong, Cobalt-nickel nanoparticles supported on reducible o:xides as Fischer -Tropsch catalysts, AC.S Catal. 10 (2020) 7343- 7354.
2. L. Liu, A. Corma, Confining isolated atoms and clusters in crystalline pornus materials for catalysis, Nat. Rev. Mater. 6 (2021) 244- 263.
3. M. Shamzhy, M. Opanasenko, P. Concepción, A. Martinez, New trends in tailoring
active sites in zeolite-based catalysts, Chem. Soc. Rev. 48 (2019) 1095- 1149.
S.-M. Wu, X.-Y. Yang, C. Janiak, Confinement effects in zeolite-confined noble metals, Angew. Chem. Int. Ed. 58 (2019) 12340-12354 .
342