J Sol-Gel Sci Technol (2012) 64:67–77DOI 10.1007/s10971-012-2828-1
Sol–gel synthesis of iron oxide–silica composite microstructures
Joanna Lewandowska•Magdalena Staszewska•
MariuszKepczynski•MichałSzuwarzyn´ski•
Anna Łatkiewicz•Zbigniew Olejniczak•Maria Nowakowska
Received: 20 April 2012 / Accepted: 26 June 2012 / Published online: 10 July 2012
©The Author(s) 2012. This article is published with open access at Springerlink.com
Abstract Spherical silica particles doped with iron oxide have been synthesized via base-catalyzed one-pot sol–gel process using tetraethoxysilane (TEOS) and iron(III) eth-oxide(ITE)asco-precursors.InthemodifiedSto¨berpro-cess adopted, depending on the concentration of ITE in the starting composition, materials of various morphologies were observed under a scanning electron microscope and an atomic force microscope. The presence of ITE signifi- cantly affected the formation process of particulate silica; the spherical particles were formed accompanied by theco- presence of irregular-shaped finer aggregates. The fraction of the aggregates with rough surfaces increased with an increase of the ITE content in the reaction mixture. Both the spherical particles and irregular-shaped aggregates contained iron hydroxide and they exhibited paramagnetic behavior. The chemical composition and physicochemical properties of the materials were determined using various complementary spectroscopicmethods.
Keywords Iron(III) ethoxide·Sol–gel·Microstructures·
Silica
1 Introduction
Over the past several years, magnetic nanoparticles of iron oxideshavegainedincreasingattentionduetothewidevariety of emerging applications of these easy to prepare biocom- patiblematerialswithfavorablemagneticproperties[1].They havebeenextensivelyexploitedasthematerialsofchoicefor magneticresonanceimaging(MRI),tissue-specificreleaseof therapeuticagentsaswellaslabelingandsortingofcells,and separationofbiochemicalproducts[2–4]forimmobilization of enzymes or controlled and targeted drug delivery [5]. However, most of these applications require nanoparticles whicharechemicallystable,uniforminsize,andformstable dispersionsinliquidmedia.Unfortunately,pristinenanopar- ticles of iron oxides tend to aggregate into large clusters, whichresultsinthelossoftheirspecificpropertiesassociated withsingle-domain,magneticnanostructures[6].Oneofthe ways to avoid these problems is a combination of magnetic nanoparticleswithothercarriers.Varietyoftheinorganicand polymericmaterialshasbeenreportedaspossiblecarriersfor magneticmaterials.Amongthemsilica,aninorganiccarrier, seems to be interesting supporting material, which can be easily prepared and retains stability in most chemical and biologicalenvironments[7,8].Ithasbeendemonstratedthat the formation of a passive coating of inert materials suchas silicaonthesurfacesofironoxidenanoparticlescouldhelpto preventtheiraggregationinliquidsandimprovetheirchem- icalstability[9].Anotheradvantageofthesilicacoatingisthat such a surface is often terminated by a silanol group, which can serve as a reacting centers allowing for covalentattach- mentofspecificligandstothesurfacesofthesemagnetic
Electronic supplementary material The online version of this article (doi:10.1007/s10971-012-2828-1) contains supplementary material, which is available to authorizedusers.
J. Lewandowska·M. Staszewska·M. Kepczynski·
M.Szuwarzyn´ski·M.Nowakowska(&)
Faculty of Chemistry, Jagiellonian University, Ingardena 3,30-060Krako´w,Poland
e-mail:nowakows@chemia.uj.edu.pl
A. Łatkiewicz
Laboratory of Field Emission Scanning Electron Microscopy and Microanalysis at the Institute of Geological Sciences of theJagiellonianUniversity,Oleandry2a,30-060Krako´w,Poland
Z. Olejniczak
Institute of Nuclear Physics, Polish Academy of Sciences,Radzikowskiego152,31-342Krako´w,Poland
13
ORIGINAL PAPER

68
J Sol-Gel Sci Technol (2012) 64:67–77
nanoparticles. That creates an opportunity to design and synthesize of magnetic carriers that can be used to deliver specific ligands to target organs via the antibody–antigen recognition [6].
Therearetwodifferentapproacheswhichhavebeenused to generate silica coatings on the surfaces of iron oxideparticles.Thefirstmethodusesthewell-knownSto¨berpro-cess [10], in which silica is formed in situ by thehydrolysis and condensation of a precursor. This method can be alsouseful for the creation of organic molecules-silica hybrid materials. In our previous work we have described the for- mationofself-assembledporphyrinmicrostructurescoveredbysilicaobtainedintheSto¨bersynthesisinthepresenceof5,10, 15, 20-tetrakis(4-hydroxyphenyl)porphyrin (mTHPP) [11]. The second method is based on microemulsion syn- thesis,inwhichsurfactantmicelleswereusedtoconfineand control the coating of silica on core nanoparticles [12]. The drawbackofthatmethodisthenecessityofseparationofthe core–shell nanoparticles from the large amount of surfac- tantspresentinthemicroemulsionsystem,whenthereaction iscompleted.
In a current paper we report on the formation of inter- esting and stable magnetic structures of micrometer size.The materials were obtained in the sol–gel synthesis car-ried out in the mixture of tetraethoxysilane (TEOS) and iron(III) ethoxide (ITE). This one-pot synthesis seem to bethe novel and attractive way in the producing the stable magnetic structure alternatively to the synthesis of core– shell Fe3O4/SiO2beads. Depending on the ITE concen- tration applied in the synthesis, the structures with different morphologies can be obtained as was shown using Atomic Force Microscopy (AFM) and Scanning Electron Micros- copy (SEM). The properties of the microstructures were characterized using thermogravimetry measurements (TG), Energy-Disperse Spectroscopy (EDS), Electron Spectros-
grade) and ammonium hydroxide (25 %, pure p.a., Chempur) were used as received. Millipore-quality water was used during the experiments.
2.2 Preparation of microstructures
Appropriate amounts of TEOS and ITE were dissolved in 6mLofethanolandthemixturewasshakenfor2days.
1.5 ml of 16 % (w/w) ammonia (obtained by mixing 1 ml of 25 % (w/w) of ammonia with 0.5 ml of water) was added to the alcoholic solution of TEOS and ITE.The sample was stirred 3 days at room temperature. Then the resulted dispersion was purified by washing with ethanol. Systems with different content of ITE in relation to TEOS were prepared. For the comparison synthesis in samples containing only TEOS or ITE were also carried out. The names and the sample composition were collected in Table1.
2.3 Scanning Electron Microscopy (SEM)
SEM observations were carried out using a cold field emission scanning electron microscope (FESEM) HIT- ACHI S-4700 equipped with a NORAN Vantage energy dispersion spectrometer. Samples for the measurements were prepared by placing a drop of solution on a silicon plate without any temperature treatment. The solvent was allowed to evaporate at room temperature andsubsequently the thin film of carbon was deposited on the sample by sputtering.
2.4 Atomic and magnetic force microscopy (AFM and MFM)
AFM and MFM images were obtained with a NanoScope IV Multimode atomic force microscope (Veeco, Santa Barbara, CA) working in the tapping mode. Standard Ve- eco silicon cantilevers for measurements in the air of normal spring constant of 40 N/m were used. Samples were prepared on silicon wafers using the spin-coating method. MFM images were acquired using the same microscope and Co/Cr covered cantilevers of normal spring constant of 2 N/m. Before scanning the cantilevers were magnetized with a small magnet. All the MFM imagesweretakeninaliftmodeat1lmlifthigh.
29Si
copy for Chemical Analysis (ESCA) and Solid-state
Magic-Angle Spinning Nuclear Magnetic Resonance Spectroscopy (29Si MAS NMR). Magnetic Force Micros- copy (AFM/MFM) application allowed us to correlate the magnetic properties with the microstructure of the mate- rials synthesized. This technique provides the interesting combination of simultaneous examination of the mor- phology and magnetic features. The conducted magnetic susceptibility and magnetization measurements character- ized the magnetic properties of the obtained material.
2.5 Magnetization measurements
2 Experimental section
The measurements of magnetization were performed at room temperature using Lake Shore 7300 vibrating sample magnetometer equipped with Stanford SR 830 lock-in nanovoltameter for controlling the current and with con- stant-flow cryostat (Janis).
2.1 Materials
Tetraethoxysilane (TEOS, C98 %, Fluka), iron(III) ethox- ide (ITE, 99 %, ABCR), ethanol (99,8 %, spectroscopic
13

J Sol-Gel Sci Technol (2012) 64:67–77
69
3 Result and discussion
Table 1 The composition (molar content of each component) of samples used in synthesis
3.1 Synthesis of microstructures
Sample
ITE/TEOS
weight ratio
Amount of TEOS (mol)
Amount of ITE (mol)
The main aim of our studies was to obtain magnetic microstructurescomposedofsilicadopedwithironatoms. For this reason the sol–gel synthesis was carried out in a mixture of TEOS and its structural analog containing Fe atoms,namelyITE.TEOSisasiliconalkoxideusedforthepreparationofsilicaparticlesintheSto¨bersynthesis[10].The synthesis results in formation of the sphericalmono-disperse silica particles in the size range from 50 nm to 2 lm. The reaction occurs in silicon alkoxide–alcohol– water–ammonia system and it is based on hydrolysisand condensation of a precursor catalyzed by ammonia.Gen- erally, it is also quite well established that the size anddistributionofsilicaparticlesformedinSto¨bersynthesisarestronglydependentonthetypeofsiliconalkoxideand alcohol used. Therefore, it was interesting to seewhether ITE can participate in the sol–gel synthesis and to deter- mineitseffectonthestructureofthenanoparticlesformed.ITEisahighlyreactivelatetransitionmetalalkoxide.This brown powder is hard to oxidize and easy to handle material.Ithasbeenpreviouslyusedasaprecursorinthe synthesis of colloidal FePt nanoparticles (NPs) [13–15]. ITE has also been used for making Fe2O3nanostructured thin films obtained by dipping silica slides in ethanolic solutions of Fe(OEt)3[16].
The reaction mixtures contained various amounts of ITE (see Table1). The content of ITE strongly affected the color of the reaction mixture, which was milky-orange for the 1 % ITE sample, brick-red for 10 % ITE sample, and dark-brown for 100 % ITE sample (Fig.1). For all samples the sedimentation was observed. Using variety of physi- cochemical methods it was demonstrated that the addition of ITE to TEOS has significant, concentration dependent, effect on morphology of the product.
1.46910-3
1.46910-3
1.46910-3
1.46910-3
1.46910-3
1.46910-3
1.46910-3
0
0 % ITE
0.1 % ITE
0.5 % ITE 1 % ITE 2 % ITE 5 % ITE 10 %ITE
100 % ITE
0
0.001
0.005
0.01
0.02
0.05
0.1
1
0
1.6910-6
0.8910-5
1.6910-5
0.32910-4
0.8910-4
1.6910-4
1.6910-3
2.6 Electron spectroscopy for chemical analysis (ESCA)
ESCA analysis was carried out using a multifunctionalESCA instrument equipped with additional equipment pro-ducedbyPREVAC.Thevacuumchamberoftheinstrument wasequippedwithan5-axialanalyticalprecisionmanipu-lator,hemisphericalchargedparticleanalyzerXPS,UPSand AES(VGScientR3000),twoanticathodalX-raytubeMg/Al(powerMg/Al400/600W),X-raymonochromator(3crys- tals) with the radiation source (a single Al anticathode. 600W),pumpingandmeasuringvacuumsystem(providedthevacuumbase\1910-8mbarafter48hannealingat150°C),thechargeneutralizinggun(FS40-PS)onthesur- faceofnon-conductingsamples(energyrange0–500eV, electron current 1–500 lA), the ion gun to perform depth profiles(IS40E-PS)andelectrongunfortheAugerspec- troscopy(ES40C-PS).ForESCAexperimenttheresulted dispersions were dried at 100°C for 24h.
2.7 Thermogravimetry measurements (TG)
Oxidation and thermal decomposition of the dried product was studied using a Mettler-Toledo TGA/SDTA851ethermogravimeter. The samples were heated at a rate of1°Cmin-1fromzeroto1,000°Cinargonandinairflowof110mlmin-1.
2.8 Solid-state29Si magic-angle spinning nuclear magnetic resonance spectroscopy (29Si MAS NMR)
29Si
MAS NMR spectra were collected on a pulse NMR
spectrometer at 59.515 MHz (magnetic field 7.05 T). A Bruker HP-WB high-speed MAS probe was used to record spectra at 7 kHz spinning speed. The ppm scale was referenced to the29Si resonance of TMS. The sample for29Si MAS NMR experiment was isolated from dispersion bydryingat100°Cfor24h.
Fig. 1 Photograph of the dispersions obtained in the sol–gel synthe- sis in samples:a1 % ITE,b10 % ITE, andc100 % ITE
13

70
J Sol-Gel Sci Technol (2012) 64:67–77
3.2 Morphology of microstructures
10 % ITE sample was used for these studies. Full-scanning ESCA spectrum of the 10 % ITE sample is shown in Fig.4a. Signals from four detectable elements (silicon, carbon, oxygen, and iron) were recorded at 103.4 (Si 2p), 285.4(C1s),532.8(O1s)andabout708–730eV(Fe2p).
The Fe 2p peak is the least detectable compared to rest of the peaks as shown in Fig.4b (high resolution ESCAspectra of Fe 2p). Some of the iron oxide structures can be identified on the basis of their core line binding energies. The small differences in the binding energy values of the core-electrons of the three oxides FeO, Fe3O4and Fe2O3have been observed since they contain FeIIand FeIIIions in
3.2.1 SEM analysis
The morphologies of synthesized materials were examined using SEM. Figure2presents the SEM micrographs for the objects obtained in the mixtures of various compositions. The individual silica particles synthesized from TEOS (in the absence of ITE) are of 445–667 nm (Fig.2a). They are of regular shapes and are quite smooth. Figure2b–g show the images for particles obtained in the presence of ITE. One can observe that ITE significantly affects the size, shape and the morphology of the obtained materials. At low content of ITE, the formation of spherical particles is accompanied by the appearance of irregular aggregate-type of materials. The fraction of the later is increasing with increase of the ITE content in reaction mixture and it is thelargestfortheproductofSto¨bersynthesiscarriedoutforITE(withoutadditionofTEOS)(Fig.2h).
Based on the SEM micrographs one could be concernedthatitisveryprobablethatduringtheSto¨bersynthesisTEOS and ITE created two different types of materials. To gain information whether the spherical objects contain the iron atoms, the energy-disperse spectroscopy (EDS) anal- ysis were carried out for samples c–g. The results were collected in the Table2. In all samples, the presence ofiron in spherical objects, as well as in aggregates was confirmed. The content of Fe in the product is dependent onthecontentofITEusedinsynthesis.
FeII
different amounts. FeO contains exclusively
ions,
which are octahedrally coordinated in a cubic lattice. Fe3O4contains both FeIIand FeIIIions in an inverse cubic spinel
FeII
FeIII
structure,withthe	ions in octahedral sitesand
ions half in octahedral and half in tetrahedral sites, whereas thea-Fe2O3contains only FeIIIions in a lattice having the rhombahedral A12O3structure. That is the reason why the binding energies of the photoelectron peaks can be used to
FeII
FeIII
provide an identification of
and
species and
of iron oxides themselves. The use of the more intense Fe 2p3/2and Fe 2p1/2peaks plus associated satellite peaks are particularly useful for that purpose [17].
In the FeO spectra the Fe
2p3/2
and Fe
2p1/2
binding
energiesareobservedat710.7and724.4eVrespectively.In a case of the Fe3O4oxide the Fe 2p3/2and Fe 2p1/2binding energy values are 710.8 and 724.7 eV, respectively. For Fe2O3theFe2p3/2peakhasabindingenergyof711.6eVand theFe2p1/2peakis725.1eV.Thesatellitepeaksoccurringat approximately 8.0 eV above the Fe 2p3/2peak is character- istic of FeIIIspecies, while the occurrence of a satellite peak at approximately 6.0 eV above the Fe 2p3/2peak is charac- teristic of an FeIIspecies [18]. In fact, the oxide species can bedistinguishedbytheabout1.0eVdifferenceintheircore line binding energies. It has been noticed that for the examinedmaterialtheSi2p,C1sandO1sarepredominant peaks. The Fe 2p spectrum is detected in spite of low intensity,asitisshownintheFig.4b.Wehaveobservedthe considerablebroadeningoftheFe2ppeaks:theFe2p3/2isin
3.2.2 AFM analysis
Atomic force microscope (AFM) measurements were done for the 100 % ITE sample and they were helpful in determination of sizes of investigated objects. Figure3showstheAFMimageoftheobjectsformedinthatsample. The results are in agreement with the described above findings from the SEM analyses. It can be seen some kind of aggregates, which are built from smaller components. The average size of the composite particles was about 8–12nminheightand30–40nminwidth,respectively.
the range of the 708–716 eV and Fe
2p1/2
are in about
721–730eV.ThemaximumvalueforFe2p3/2peakisabout
3.3 ESCA analysis
711.9 and 725.6 eV for Fe
2p1/2
peak which might be
assigned to the presence of the Fe2O3oxide. Nevertheless, takingintoaccounttheverysmallchangesinbindingenergy of the above mentioned iron oxide structures on the basisof thepresentedESCAspectraitisdifficulttoidentifyprecisely the kind of Fe species, which are formed duringsynthesis.
Because of the interesting morphology obtained in the case of the system 1 % ITE we have decided to study properties of that material more carefully. The TG, ESCA analysis and some magnetic measurements have been done to characterize that structure.
ESCA was used to reveal the changes in chemicalcompositionoftheITE,whichoccurredduringSto¨bersynthesis. ESCA spectrum for 1 % ITE sample was diffi- cult to interpret because of the low iron content. Thus, the
3.429Si MAS NMR analysis
To gain more insight into the chemical structure of the obtained material29Si MAS NMR technique was applied.
13

J Sol-Gel Sci Technol (2012) 64:67–77
71
Fig.2SEMmicrographsofthematerialsobtainedinSto¨bersynthesisintheTEOS-ITEsystems:a0%ITE,b0.1%ITE,c0.5%ITE,d1%ITE, e 2 % ITE, f 5 % ITE, g 10 % ITE, h 100 % ITE
differ from each other. The integrated peak area of the29Si spectrum for 2 and 5 % ITE samples represent 70 and 55 %, respectively, of that characteristic for peak area of 0 % ITE sample. Because the amount of TEOS used in synthesis was the same for all samples the numberof
Spectra obtained for 0, 2, and 5 % ITE samples are shown in Fig.5. Because of the strong magnetism it was not possible to analyze sample with higher content of iron oxide. For all these samples the observed signals are located at the same chemical shift but their intensities
13

72
J Sol-Gel Sci Technol (2012) 64:67–77
and the signal becomes beyond detection. This broadening takes place only if the distance between iron and silicon atoms is not large. That might suggest that at low tempera- ture,evenintheabsenceofFe–O–Sibonds,theinteractions betweenSiandFecanoccurthroughSiOHgroupspresentat thematrixsurface.WehavealsocarriedouttheFTIRstudies (the supplementary figure) but have not observed thesignal whichcouldbeascribedtoFe–O–Sibond.Onthebasisofthe above mentioned findings we have postulated that our syn-thesis resulted in formation of the materials in which the silica particles with –OH groups at the surface interact with iron oxide species. The distance between them are small enoughtocausethechangeswhichwehaveobservedin29Si MAS NMR spectra.
Table 2 Weight content of iron in samples obtained experimentally (EDS measurements) and calculated
Sample
%wt. Fe exp
%wt. Fe calc
10 % ITE
5 % ITE
2 % ITE
2.32±0.25
1.61±0.11
0.51±0.08a
0.25±0.10b
0.47±0.08a
0.38±0.09b
0.16±0.10a
0.22±0.10b
2.66
1.39
0.57
1 % ITE
0.29
0.5 % ITE
0.15
a
Material organized into spherical particles
Material with irregular shape
b
3.5 Calcination
silicon atoms can be assumed to be
the same in
each
29S
product. The loweringofthe	integrated peak areain
To determine whether the properties of obtained materials have changed after heat treatment for sample 1 % ITE the calcination was performed. The sample was calcinated on the silica plates in argon and in air atmosphere, respec-
tively. The calcination was performed in 600°C, with the10°Cmin-1rate.SEManalysesforthecalcinationprod-ucts were conducted. Figure6presents the SEM images
before and after calcination. Further condensation of the silica matrix had occurred on heating. After calcination the siloxane network is more highly condensed and more highly ordered, but there are no observable changes in themorphology. The energy-disperse spectroscopy (EDS) analysis was carried out and the results did not show any noticeable differences.
samples containing the iron species reflect their effect on silicon atoms.
Brunietal.[19]haveinvestigatedtheinteractionsofiron oxidewiththesilicamatrixinaFe2O3–SiO2nanocomposite prepared by a sol–gel method and subsequently annealed at hightemperature(upto900°C).UsingNear-,Mid-,andFar- IR,29SiMAS-and1HNMRtechniquestheyhaveshownthat the Fe2O3nanoparticles interacted with the silica or silanol groupsatthesurfaceofthecavitiesinwhichtheywereform. These authors have noticed that for the nanocomposite treated at higher temperature the integrated peak area ofthe29SispectrumdecreasedandintheMid-IRspectratheyhaveobservedthesignalat590cm-1indicatingformationofFe–O–Si bonds at the nanoparticle-matrix interface. Addition- ally, they have also shown that some kind of interactions between iron oxide nanoparticles and silica matrix operate even at low temperature. However, due to the presence of iron (III) paramagnetic ions in close proximity to the Si atoms, the29Si signal broadens while its intensitydecreases
3.6 TG measurements
It is well established that there are two distinct mass loss steps in the thermograms of silicas. The first step is mainly
Fig.3AFMmicrographsmaterialobtainedasaproductofSto¨bersynthesisinthe100%ITEsample.a3Dimageofthesurface,bcross-sections
13

J Sol-Gel Sci Technol (2012) 64:67–77
73
Fig. 529Si MAS NMR spectra of the 0 % ITE, 2 % ITE and 5 % ITEsample
considerable decrease in the amount of isolated hydroxyls, but for the complete removal of the rest of silanols, the temperatures has to be higher than 1,200°C [20].
The thermograms for the 1 % ITE sample are depicted in Fig.7. TG profiles have been obtained in oxidative and inert atmosphere. In both cases three steps of the mass losses have been observed. TG profile in oxidative atmo- sphere shows onset of oxidation at about 60°C. First rapid oxidation step accounts for 2.1 % of total 10.2 % massloss,thesecondstepisatabout250°Candaccountsfor
4.0 % mass loss and the last one occurs at about 500°C
with mass loss of 4.1 %. TG profiles obtained in inert atmosphere show very similar decomposition and desorp- tion. We observed three steps of the mass loss: at 60°C (1.8%),250°C(4.2%)andabout525°C(4.8%).Total
mass loss in an inert atmosphere accounts for about
10.8 %.
Based on the literature, we can assume that the first step of decomposition is associated with the removal of
Fig. 4 ESCA spectra of: a full scan, b high-resolution of Fe 2p of the 10 % ITE sample
connected with the removal of the physically adsorbed water from the silica surface, whereas the second step is due to slow condensation of silanols. The temperature where physically adsorbed water was considered to be completely released was found to be in the range from 100 to 130°C and was dependent on the type of silica [20]. However, according to Zhuravlew [21] the temperature corresponding to the ending of dehydratation and the beginning of dehydroxylation is in the range of 190±10°C, which means that small amount of physi- cally adsorbed water remains at the sample surface up to 200°C. Heating of the silica samples at 1,100°C resultsin
Fig. 6 SEM micrographs of the 1 % ITE sample after calcination in: a air atmosphere, b argon atmosphere
13

74
J Sol-Gel Sci Technol (2012) 64:67–77
Takingintoaccounttheaboveinformationwecanassume that the concentration of ITE in analyzed sample was high enough to affect the TG profile of the silica matrix. Thethermal-treatment removes the volatile substances and simultaneously causes the densification of silica matrix along with the formation of some iron oxidenanoparticles.
3.7 Magnetic measurements
3.7.1 MFM analyses
Magneticforcemicroscopytechnique(MFM)wasusedto confirm magnetic properties of the samples. Microscope worked in interleave mode scanning all points onsample twice—inthetappingmodetoobtainAFMtopographyand phaseimagesandintheliftmode(1lm)toobtainpicturesof MFMphase[24].Theimagesobtainedfor1%ITEsample, 1%ITEaftercalcinationinargonandairareshowninFig.8. Itwasconfirmedthatallofthemaremagneticmaterials.
Thereisvery good correlations betweenAFM andMFM images (Fig.8a–c)for allsamples.Theaggregates shown onAFMtopographyandphase images reveal contrast alsoinmagnetic mode (MFM), which occurs onlyformagnetic sam-plewhich interactswith tip. Thatsuggeststhematerial shows homogeneous distributionofthe ironoxide withinthesample.
Fig. 7 TG profiles obtained in oxidative and inert atmosphere for 1 % ITEsample
physically adsorbed water and solvents used in the syn- thesis. Although the sample before TG experiments was dried at 100°C, it is possible that the some amounts of the mixture of water, ethanol and ammonium were still trapped in the material before the TG experiment. The continuation of the thermal treatment causes the condensation of silanolgroups of the silica surface resulting in the release of water and formation of siloxane group. The dehydratation and dehydroxylations reactions overlap to some extent so it is difficult to define the remarkable border between each of them. In fact, the TG profile for our sample differs from that observed in typical experiment for the silica. That reflects the presence of iron compound produced duringSto¨bersynthesis.
Barick et al. [22], in his work on fabrication of com- posite materials in situ generation ofc- ande-Fe2O3nanoparticlesinaSiO2matrixthroughsol–gelprocess,has foundthatTGprofilesarestronglydependentonthecon- centration of Fe3?. He has observed two main steps of thermal decomposition for samples with lower Fe3?con- centration(x=0.05and0.1)andthreestepsforsample
3.7.2 Measurements of magnetic susceptibility
Oneofthevaluewhichcharacterizesthemagneticfeatures ofthematerialisthemagneticsusceptibility(v).Inthecaseoftheparamagneticmaterialsthevalueofmagneticsus- ceptibilityv[0, whereas for diamagnetic substancesv\0(v=0invacuum)[25].Forexample,themagneticsusceptibility for paramagnetic materials is in therange:
?0.65910-6emu/gforaluminium,?106.37910-6emu/gforoxygen.Fordiamagneticmaterialsthevalueforcopperisequal–0.09910-6emu/gandforsilicon
–0.13910-6emu/g[26].
Figure9shows the magnetic susceptibility for our sample obtained in system containing 1 % ITE. The magnetic susceptibility value for that sample was found tobeequalto5.01910-6emu/g-sample,whichisintherange characteristic for paramagnetic material. That small value of magnetic susceptibility is due to the low contentof iron in the sample. Nevertheless the magneticsusceptibility calculatedfor1gofironpresentinthesampleisequal
1.73910-3emu/g-Fe.
Fe3?
with higher
concentration (x=0.2). The alcogel
samples exhibit significant weight loss in the low temper- ature range (25–100°C) mainly assigned to the removal of solvent (water and ethanol absorbed into the matrix). The thermal decomposition in the temperature range of 100–1,000°C was explained by the evolution of organic species and structurally bonded –OH groups. For samples with the highest content of Fe3?these authors observed the thermal decomposition in the temperature range of 100–235°C which was accompanied with an exothermic effect at 224°C assigned to the formation ofc-Fe2O3from the thermal decomposition ofc-FeOOH originally formed during sol–gel synthesis [23].
3.7.3 Magnetization measurements
In order to compare the magnetic properties of our material with these determined for iron oxides-silica composites reported in literature [22,27] we have performed the
13

J Sol-Gel Sci Technol (2012) 64:67–77
75
Fig. 8 Images of AFM:
a topography, b AFM phase and c corresponding MFM phase ofSto¨bersynthesisproductsfor
1 % ITE sample (1), the same sample after calcination in argon (2) and sample after calcination in air (3)
additional magnetization measurements. Figure10pre- sents magnetization curves for the 1 % ITE sample. The curve has a symmetrical sigmoid shape—when the mag- netic induction decreased, the magnetization decreased and eventually reached zero, no hysteresis is observed. Nev- ertheless the material does not exhibit saturation behavior up to a maximum magnetic induction used in the experi- ment. There was only possible to determine the maximum magnetization which is equal 0.028 emu/g-sample, what translates to 10.01 emu/g-Fe. It has been demonstrated previously that the magnetization of core–shell super- paramagnetic Fe3O4/silica nanoparticles have reached the saturation [27]. The value of the saturation magnetiza- tion for pristine Fe3O4nanoparticles is about 60.5 emu/g– Fe3O4(which can be expressed as a 83.6 emu/g-Fe) whereas for core–shell magnetite/silica composite particles with 17.3 wt. % of magnetite that value decreasedto
Fig. 9 The results of magnetic susceptibility measured for the 1 % ITE sample using a magneticbalance
13

76
J Sol-Gel Sci Technol (2012) 64:67–77
7.5 emu/g-sample (59.6 emu/g-Fe) [27]. It has been shown also that coating of magnetic particles with non-magnetic materialssuchassilicainfluencesthevalueofmagnetization due to the quenching of surface moments [28]. The thicker silica shell—the lower the saturation magnetization[8].
Barick et al. [22] reported on the preparation of dis- persed iron oxide Fe2O3nanoparticles in silica matrix using sol–gel process. The resulting samples contained various amounts of iron oxide. The synthesized samples were thermally annealed. Magnetization measurements have shown that all samples exhibit non-saturation behavior up to a maximum field of 20 kOe. The observed maximum magnetization for samples treated at 800°C was equal: 0.27, 0.38 and 1.23 emu/g-sample depending on the Fe3?concentration. The authors have explained the low values of maximum magnetization by taking into account thepresence of large amount of non-magnetic SiO2matrix. The lack of the saturation has been interpreted as resulting from a coexistence of fraction of superparamagnetic par- ticles with ferri/ferromagnetic coupledparticles.
Taking into account the above mentioned studies we can concluded that maximum magnetization value of the 1 % ITE (0.028 emu/g-sample) is about ten times lower than that presented in Barick studies [22] for the smallest iron oxide content (0.27 emu/g-sample). That reflects the highcontent of silica in our material. To make a comparison of our results with these presented in literature we haveexpressed magnetization in units emu per gram of ironpresent in the samples. The value obtained for 1 % ITE sample was found to be 10.01 emu/g-Fe and it is of the same order of magnitude as that presented in the litera- ture—59.6 emu/g-Fe [27].
Our material is attractive as it can be obtained using a simpleone-potsyntheticstrategy.Additionally,evenifonly 1 % wt. of ITE was used in synthesis the process resulted in preparation of material with magneticproperties.
Furthermore our synthetic strategy can be used for prepara- tion of other types of magnetic composite microstructures.
4 Conclusions
Thesilicamaterialscontainingvariousamountsofironoxide incorporatedwereobtainedfromTEOSandITEmixturesintheSto¨bersynthesis.ThepresenceofironinallmaterialssynthesizedwasconfirmedbyEDSanalyses.Themorphology ofthesematerialsisstronglydependentontheamountofFe present. The SEM micrographs and AFM measurements indicated that at low Fe content the formation of regular, spherical particles is accompanied by the appearance of irregularaggregate-typeofmaterials.Thefractionofthelater isincreasingwithincreaseoftheFecontentinreactionmix- ture. TG analyses indicated that even small amount of iron present in the particles can affect their thermal behavior. ESCA analysis has not provided an unambiguous answer concerning the creation of defined phase of iron oxide.29SiMAS NMR spectra have suggested that obtained materials consistofsilicananoparticleswhichinteractedwithironoxidespecies. MFM, magnetic susceptibility and magnetization measurements have demonstrated that our materials have magnetic properties. Values of magnetic susceptibilityindi- cated that the material is paramagnetic. The magnetization measurementshaverevealedthatsampleobtainedinapres- ence of 1 % ITE did not exhibit saturation behavior up to a maximummagneticinductionused.Thehighcontentofsilica in our material has affected the maximum magnetization value which was equal to 0.028 emu/g-sample, what trans- lates to 10.01 emu/g-Fe. MFM experiment suggests thatthe homogenous distribution of iron oxide in the silica matrix obtained. Overall, it can be concluded that even the small content of ITE (1 %wt) in the reaction mixture resulted in formation of the paramagnetic materials. It is, however, expected that the material with more homogeneous mor- phology would show better properties. The studies aimedat obtainingsuchmaterialsarecurrentlyinprogress.
Acknowledgments This work was supported by the European Union from the resources of the European Regional Development Fund under the Innovative Economy Programme (grant coordinated by JCET-UJ, NoPOIG.01.01.02-00-069/09).
Open Access This article is distributed under the terms of the Creative Commons Attribution License which permits any use, dis- tribution, and reproduction in any medium, provided the original author(s) and the sourceare credited.
References
1. Morales MA, Mascarenhas AJS, Gomes AMS, Leite CAP, Andrade HMC, de Castilho CMC, Galembeck F (2010) J Colloid Interface Sci 342:269–277
Fig. 10 Magnetization curves in a function of magnetic induction for the 1 % ITE sample
13

J Sol-Gel Sci Technol (2012) 64:67–77
77
1. Babes L, Denizot B, Tanguy G, Jacques J, Jeune L, Jallet P (1999) J Colloid Interface Sci212:474–482
2. Xu ZP, Niebert M, Porazik K, Walker TL, Cooper HM, Mid- delberg APJ, Gray PP, Bartlett PF, Lu GQ (2008) JControl Release130:86–94
3. Fornara A, Johansson P, Petersson P, Gustafsson S, Quin J, Olsson E, Ilver D, Krozer A, Muhammed M, Johansson C (2008) Nano Lett8:3423–3428
4. Chen F, Shi R, Xue Y, Chen L, Wan Q-H (2010) J Magn Magn Mater322:2439–2445
5. LuY,YinY,MayersBT,XiaY(2002)NanoLett2:183–186
6. Wang Ch, Yan J, Cui X, Wang H (2011) J Colloid Interface Sci 354:94–99
7. Sun X, Liu F, Sun L, Wang Q, Ding Y (2012) J Inorg Organomet Polym22:311–315
8. Butterworth MD, Illum L, Davis SS (2001) Colloids Surface A 179:93–102
9. Stober W, Fink A, Bohn E (1968) J Colloid Interface Sci 26: 62–69
10. Staszewska M, Dzieciuch M, Lewandowska J, Kepczynski M, Zapotoczny S, Oszajca M, Łatkiewicz A, Nowakowska M (2011) J Sol-Gel Sci Technol59:276–282
11. Santra S, Tapec R, Theodoropoulou N, Dobson J, Hebard A, Tan W (2001) Langmuir17:2900–2906
12. SaitaS,MaenosonoS(2005)ChemMater17:3705–3710
1. SaitaS,MaenosonoS(2005)ChemMater17:6624–6634
2. Maenosono S, Suzuki T, Saita S (2008) J Magn Magn Mater 320: L79–L83
3. Armelao L, Granozzi G, Tondello E, Colombo P, Principi G, Lottici PP, Antonioli G (1995) J Non-Cryst Solids 192&193: 435–438
4. Mills P, Sullivan JL (1983) J Phys D Appl Phys16:723–732
5. Iijima Y, Miyoshi K, Saito S (1999) Surf Interface Anal27:35–42
6. Bruni S, Cariati F, Casu M, Lai A, Musinu A, Piccaluga G, Solinas S (1999) Nanostruct Mater11:573–586
7. Ek S, Root A, Prussa M, Niinisto L (2001) Thermochim Acta 379:201–212
8. ZhuravlewLT(1993)ReactKinetCatalL50:15–25
9. Barick KC, Varaprasad BSDChS, Bahadur D (2010) J Non-Cryst Solids356:153–159
10. Yen FS, Chen WC, Yang JM, Hong ChT (2002) Nano Lett 2:245–252
11. Moskalenko AV, Yarova PL, Gordeev SN, Smirnov SV (2010) Biophys J98:478–487
12. Gupta AK, Gupta M (2005) Biomaterials26:3995–4021
13. http://info.ee.surrey.ac.uk/Workshop/advice/coils/mu/#sus
14. Kobayashi Y, Saeki S, Yoshida M, Nagao D, Konno M (2008) J Sol-Gel Sci Technol45:35–41
15. Xu H, Tong N, Cui L, Lu Y, Gu H (2007) J Magn Magn Mater 311:125–130
13