Jagiellonian University
Jagiellonian University Institute of Physics
Department of Statistical Physics
Doctoral thesis
Lattice
Models of Biaxial, Tetrahedratic and Chiral Order
Karol Trojanowski
Supervised by prof. dr hab. Lech Longa
Cracow, Summer 2013

ii

iii
Peer-reviewed papers
Karol Trojanowski, David W. Allender, Lech Longa and Łukasz Kuśmierz. (2011).
Theory of Phase Transitions of a Biaxial Nematogen in an External Field. Molec- ular Crystals and Liquid Crystals, 540(1), 59-68.
•
Karol Trojanowski, Grzegorz Pająk, Lech Longa and Thomas Wydro.	(2012).
Tetrahedratic mesophases, chiral order, and helical domains induced by quadrupo- lar and octupolar interactions. Physical Review E, 86(1), 011704.
•
Lech Longa and Karol Trojanowski. (2013). Ambidextrous Chiral Domains in
Nonchiral Liquid-crystalline Materials. Acta Physica Polonica B, 44(5), 1201-1207.
•
Karol Trojanowskia and Lech Longa. (2013). Synchronization of Kuramoto Oscil-
lators with Distance-dependent Delay. Acta Physica Polonica B, 44(5), 991.
•
Conference talks and posters
March 2009. 35th Conference of the Middle European Cooperation in Statisti-
cal Physics, Pont-a-Mousson, France. Poster “Synchronization of Phase-coupled Oscillators With Distance-dependent Delay”.
•
July 2010. 23rd International Liquid Crystal Conference, Kraków, Poland. Poster
“Biaxial phase of interacting quadrupoles in an external field”.
•
February 2011. 11th European Conference on Liquid Crystals, Maribor, Slovenia.
Oral presentation “Biaxial phase in nematic liquids under influence of external fields”.
•
September 2011. 24th Marian Smoluchowski Symposium on Statistical Physics,
Zakopane, Poland. Poster “Effects of external fields in the interacting quadrupoles model of biaxial nematics”.
•
November 2011. 12th International NTZ-Workshop on New Developments in Com-
putational Physics, Leipzig, Germany. Oral presentation “Frequency-locking and pattern formation in the Kuramoto model with Manhattan delay”.
•
September 2012. 25th Marian Smoluchowski Symposium on Statistical Physics,
Kraków, Poland. Poster “Lattice simulations of tetrahedratic and chiral order”.
•

iv
March 2013. 38th Conference of the Middle European Cooperation in Statistical
Physics, Trieste, Italy. Poster “Tetrahedratic mesophases, chiral order, and helical domains induced by quadrupolar and octupolar interactions”.
August 2013. 26th Marian Smoluchowski Symposium on Statistical Physics, Kraków,
Poland. Oral presentation “Frequency-locking and pattern formation in the Ku- ramoto model with Manhattan delay”.
September 2013. 13th European Conference on Liquid Crystals, Rodos, Greece.
Oral presentation “Chiral structures of nonchiral liquid- crystalline materials”.

v
Abstract
The developments over recent years in the research of liquid crystals with non-standard
symmetry fuel intensified endeavors, as scientists turn their attention to exotic liquid crystal compounds, such as bent-core mesogens, ferrocene mesogens and, recently, flexible dimers, which, according to many reports, produce phases unlike anything studied before. Among the most notable properties of these phases is ambidextrous chirality – where in the nematic phase the sample forms domains of opposite handedness. Furthermore, the biaxial nematic phase continues to garner interest. This phase had been long missing, but has been supposedly discovered in a bent-core liquid crystal in 2004 – a finding which was subsequently criticized, but spurred a heated dispute over the experimental feasibility of stabilizing the biaxial nematic phase, which has also lead to discussion whether the phase could be field-stabilized (and if this was actually the case in the famous experiments). Further results hint also at long-range tetrahedratic ordering and the curious phenomenon of spontaneous chiral symmetry breaking and forming of chiral twisted macroscopic states. The twist-bend nematic phase, which has been recently discovered for flexible dimers, appears to exhibit helical-conical twists of pitch at the nano-scale, apparently spanning only several molecules, which is particularly surprising, since in most of the chiral phases, such as the cholesteric phase, the pitch is hundreds to thousands of molecules long. Since a satisfying theoretical account of these effects in the form of a microscopic model has not been yet given, the present thesis aims to recreate these phenomena in the framework of a generalized lattice dispersion model, studied by Monte Carlo simulations and by application of mean-field theory.
After a general introduction to liquid crystals and their symmetries in Chapter 1, in
Chapter 2 the model is defined through the formalism of symmetrized irreducible spher- ical tensors, which we use as symmetry-adapted building blocks. In the dispersion inter- action potential, which can be represented as coupling of molecular multipolar moments of two molecules, we consider the molecular quadrupolar moment Q(Ωˆ ), which consists of a cylindrically-symmetric uniaxial part and a biaxial part of rectangular-cuboidal
symmetry, and the molecular octupolar moment T(3), which is a spherical tensor of the
2
symmetry of a regular tetrahedron. Two intermolecular coupling terms are constructed out of the respective multipolar moments involving coupling of moments of the same order exclusively. Additionally, a term quadratic in a generalized external vector field is introduced, where the molecular diamagnetic or dielectric polarizability tensor is as- sumed proportional to the molecular quadrupolar moment. Finally, two terms which account for coupling of the quadrupolar and octupolar moments to the intermolecular
vectors are proposed. The full Hamiltonian considers intermolecular interaction between

vi
nearest neighbors on a simple cubic lattice with periodic boundary conditions. This gen-
eral model is subsequently studied in three limit cases, the model of a biaxial nematic in an external field in Chapter 3, the model with quadrupolar and tetrahedratic octupo- lar coupling terms in Chapter 4 and its extension to intermolecular vector coupling in Chapter 5.
The first considered case, which is the model of a biaxial nematic in an external field,
can be regarded as an extension of a well-known model, which was studied extensively by Luckhurst and Romano, who built up from the pioneering work of Freiser in 1970 and Straley in 1974. This model is known to produce the Maier-Saupe transition from the isotropic to the uniaxial nematic phase, as well as a low-temperature second-order transition to the biaxial nematic phase. In the parametrization which we use, a scalar parameter λ mixes two symmetrized irreducible tensors, which correspond to uniaxial and biaxial symmetries to compose the molecular quadrupolar moment Q(Ωˆ ) – a second- rank symmetric and traceless tensor. Q(Ωˆ ) can be regarded as the anisotropic part of the molecular (dielectric or diamagnetic) polarizability tensor and varying λ represents modulating the shape of the molecule. The spectrum of λ covers shapes from uniaxial prolate (rodlike) to uniaxial oblate (discotic) molecules, with biaxial shapes of either tendency in between. A symmetry transformation of the Luckhurst-Romano model exists between the prolate and oblate sides of the range of possible values of λ, with a pivot point at a special value, called the self-dual point (at which the model is symmetric with itself), which also corresponds to completely (maximally) biaxial molecules (ones which cannot be unequivocally classified as either prolate or oblate). By an addition of a term quadratic in field and linear in Q(Ωˆ ) to this model, we study the field-induced effects on the bulk sample of mesogens which exhibit interactions of uniaxial and biaxial symmetry.
Firstly, the effects of arbitrary non-zero field are predicted through considering the min-
imum of the field interaction potential in all phases, for both cases of anisotropy of the molecular polarizability (positive or negative) and with respect to varying λ. This analysis reveals a duality transformation of the model which involves switching the sign of molecular anisotropy and the shape tendency (shifting λ about the self-dual point) simultaneously, thus linking the effects encountered for prolate molecules with positive molecular anisotropy to those encountered for oblate molecules with negative molecu- lar anisotropy and, conversely, those encountered for prolate molecules with negative anisotropy to effects present for oblate molecules with positive molecular anisotropy. In the last two cases the field induces biaxiality in the nematic phase. The field effects at the self-dual point need to be treated separately because of the high symmetry involved.
Subsequently, the phase diagrams of the model are studied in the space of the temperature
and a field parameter, which is the product of the squared field magnitude and the

vii
molecular anisotropy. (This allows us to consider the cases of positive and negative
anisotropy and varying field magnitude on the same phase diagram by using only one parameter.) The isotropic to uniaxial nematic phase transitions terminates at a critical point for prolate molecules of positive molecular anisotropy and for oblate molecules of negative molecular anisotropy, as the field is increased. For the remaining cases the transition is made continuous at a tricritical point for a sufficiently large magnitude of the field. Using a mean-field high-temperature expansion the critical and tricritical points are studied. Values of critical field and critical temperature are found for both cases in the entire molecular shape spectrum, parametrized by λ. The main result states that when the self-dual point is approached from either side (the molecular biaxiality is increased), the critical field for both the critical and tricritical points is lowered and is zero at the self-dual point. The critical temperature for the both cases is found to increase with λ. Mean-field calculations and Monte Carlo simulations are carried out for selected values of λ and at the self-dual point to study the exemplary phase diagrams for the model in detail. As expected on the grounds of the duality transformation, the shapes of the phase diagrams for prolate and oblate molecules are mutually inverted with respect to the field parameter. In both cases the temperature of the isotropic to uniaxial nematic phase transition is increased with field. The biaxial phase and the transition temperature is not altered by the increased field in the cases of prolate molecules of positive molecular anisotropy and for oblate molecules of negative molecular anisotropy, while for the remaining cases the biaxial phase is also induced in the uniaxial nematic phase and the zero-field transition to the biaxial nematic phase is removed. For maximally biaxial molecules (for λ at the self-dual point) the external field works to reduce the temperature of the transition to the biaxial phase (for either case of molecular anisotropy), which is the only case of field-lowering of the transition temperature for this model.
The lattice dispersion model with quadrupolar and tetrahedratic octupolar coupling
terms was originally postulated by Longa, Pająk and Wydro [1] and our aim here is to extend the research by providing detailed analysis in the terms of temperature scans of order parameters, fluctuation of energy and order parameter susceptibilities for some of the cases which have not been yet considered. In Chapter 4 we study the model for representative values of λ (including the self-dual point) and for two cases of the coupling constant which scales the tetrahedratic interaction term, τ . The first case corresponds to a phase diagram dominated by nematic phases, already obtained in [1], but for which no temperature dependence of the order parameters and susceptibilities has been previously given. The second case leads to a phase diagram with a multicritical point at which six phases: isotropic, nematic uniaxial oblate, tetrahedratic, nematic tetrahedratic prolate, nematic tetrahedratic oblate and chiral nematic tetrahedratic meet. The results for the

viii
nematic-dominated phase diagram corroborate the previous result from [1]. The biaxial
nematic phase exists only in the vicinity of the self-dual point, while away from it there exist sequences of isotropic, nematic uniaxial, nematic tetrahedratic and chiral nematic tetrahedratic phases, with decreasing temperature. The phase transitions associated with spontaneous breaking of tetrahedratic symmetry are manifestly first-order and the phase transitions to the biaxial nematic and chiral phases are second order. For the second case, for which the multicritical point is found, there exists a direct first-order phase transition from the isotropic phase to the chiral nematic tetrahedratic phase at the self- dual point. For the remaining cases the expected purely tetrahedratic phase is not found, as it exists in a too narrow temperature range. Instead, a sequence of phases is found of isotropic, nematic tetrahedratic and chiral nematic tetrahedratic phases, with lowering temperature. As before, the isotropic to nematic tetrahedratic phase transition is first order, while the nematic tetrahedratic to chiral nematic tetrahedratic phase transition is second-order. The chiral nematic tetrahedratic phase is not only chiral, but also spatially homogeneous and biaxial. This might come across as counter-intuitive, as chirality is known to lead to inhomogeneous ground states. However, this model does not explore all of the couplings which can be constructed with the tensors present in the theory.
In particular, an antisymmetric tensor can be constructed out of the tetrahedratic oc-
tupolar molecular tensor and the uniaxial and biaxial parts of the molecular quadrupo- lar tensor. This leads to the interaction terms involving coupling of the quadrupolar and octupolar tensors to intermolecular lattice vectors, considered in Chapter 5. The quadrupolar version of this interaction is inserted into the model with quadrupolar and tetrahedratic octupolar coupling. The resulting model is given a preliminary investiga- tion, consisting mainly of simulation results in the form of configuration snapshots and commentary. Firstly, a basic discussion of the ground state of the interaction poten- tial leads to a conclusion that the minimum is achieved when two neighboring particles are rotated with respect to each other. This is demonstrated by simulation on a one- dimensional chain. We follow with a discussion on how the ground state in two and more dimensions leads to frustration, which results in the formation of complex structures. Simulations on a two-dimensional lattice show that there exists a phase transition from the disordered to the chiral phase (this is the only phase transition in two dimensions, as other degrees of freedom are continuous), in which there appears to be some kind of reordering and two distinct types of structures are present in the lower and higher tem- perature regimes. One is identified as a bent-wavefront-cholesteric structure, in which cholesteric-like layers bend at right angles, but form no defects. The second is a simpler layered structure, akin to a two-dimensional cholesteric. In three dimensions we have also identified two distinct structures in the chiral phase, out of which the low-temperature one is an unidentified complex supramolecular structure, while in the high-temperature

ix
structure the molecules form helical twists in a layer-like structure with a pitch spanning
only several molecules. In this case the bulk cross-sections bear an uncanny resemblance to the freeze-fracture patterns only recently obtained in experiments on the twist-bend nematic phase.
In the final chapter we comment on the entirety of the obtained results and on the many
cases which have not been investigated in this thesis.

Acknowledgements
The Monte Carlo simulation software used in this work is partly inspired by the software
originally written by Tomasz Wydro.
This work is supported by the International PhD Projects Programme of the Foundation
for Polish Science within the European Regional Development Fund of the European Union, agreement no. MPD/2009/6.
The research was carried out with the supercomputer “Deszno” purchased thanks to
the financial support of the European Regional Development Fund in the framework of the Polish Innovation Economy Operational Program (contract no. POIG.02.01.00-12- 023/08).
x

Contents
Papers and conference appearances
iii
Abstract
v
Acknowledgements
x
1
Introduction
1
1
2
3
4
6
8
9
9
11
11
13
15
15
17
19
20
1.1
Liquid crystals, typical phases and symmetries
. . . . . .
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
1.1.1
1.1.2
Typical thermotropic mesophases and symmetries .
Molecular chirality . . . . . . . . . . . . . .
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
1.2
1.3
1.4
1.5
Non-standard phases . . . . . . . . . . . . . . . . .
Introduction to order parameters in liquid crystals Dispersion forces . . . . . . . . . . . . . . . . . . .
Historical results . . . . . . . . . . . . . . . . . . .
1.5.1
1.5.2
Maier-Saupe model of thermotropic nematics (lattice case) .
Lebwohl-Lasher lattice model
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
1.6
1.7
1.8
Alignment tensor . . . . . . . . . . .
Mean-field theory for lattice models . Monte Carlo simulations . . . . . . .
1.8.1
1.8.2
1.8.3
Metropolis algorithm . . . . .
Rotational degrees of freedom
Parallel sampling and pseudorandom number generation
1.9
Purpose and plan of thesis . . . . . . . . . . . . . . . . . . . . .
2
Generalized dispersion model for bent-core (and related) systems
2.1	Irreducible tensors and symmetrization . . . . . . . . . . . . . . . . .
23
23
25
26
.
.
.
.
.
.
.
.
.
2.1.1
Symmetrized irreducible tensors for selected symmetry groups
2.2	Definition of the model . . . . . . . . . . . . . . . . . . . . .
.
.
.
.
.
3
Dispersion model of biaxial nematics in an external field
31
31
31
32
34
36
36
38
3.1
3.2
Introduction . . . . . . . . . . . . . . . . . . . . . . .
Dispersion models of biaxial nematics	. . . . . . . .
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
3.2.1
Dispersion model of interacting quadrupoles .
Properties of Q(Ωˆ ) . . . . . . Duality transformation . . . Phases and phase transitions
3.2.1.1
3.2.1.2
3.2.1.3
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
3.3
Dispersion model with external field . . . . .
xi

Contents
xii
3.3.1
3.3.2
Model . . . . . . . . . . . . . . . . . .
Field-induced effects . . . . . . . . . .
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
39
39
40
41
42
42
43
43
43
45
45
46
47
48
48
50
52
58
58
59
61
63
64
72
74
78
78
78
79
79
80
3.3.2.1
3.3.2.2
3.3.2.3
Uniaxiality-promoting effects
Biaxiality-promoting effects
.
.
.
.
.
.
1
Field effects for λ =	.
.
.
.
.
.
√6
.
.
.
.
3.3.3
Duality transformation .
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
3.4
Tools and methods . . . . . . .
3.4.1
Order parameters . . . .
3.4.1.1
3.4.1.2
3.4.1.3
Alignment tensor .
Definition of order parameters
Invariant parameter w .
.
.
.
.
.
.
.
.
.
.
.
.
.
.
3.4.2
Mean-field method . . . . . . . .
3.4.2.1
3.4.2.2
Self-consistent approach
High-temperature expansion
3.4.3
Monte Carlo simulations . . . . . . . .
3.4.3.1
Specific heat and susceptibilities
3.5
3.6
Results for the Luckhurst-Romano model	.
Studying the model with external field . . .
.
.
.
.
.
.
.
.
.
3.6.1
Critical and tricritical points	. . . .
3.6.1.1
3.6.1.2
3.6.1.3
Mean-field calculation of the critical point
Mean-field calculation of the tricritical point
Conclusions and comments on simulations and experiment
3.6.2
3.6.3
3.6.4
Results for λ = 0.3
Results for λ = 0.5
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
1
Results for λ =
√6
3.7
Summary . . . . . . . . .
3.7.1
Phase diagrams and order parameters
3.7.1.1
3.7.1.2
3.7.1.3
3.7.1.4
λ = 0.3
λ = 0.5
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
1
λ =
√6
Mean-field study of critical and tricritical points
4
Tetrahedratic order and chiral symmetry breaking in a dispersion model
of liquid crystals
81
81
82
84
85
87
88
89
89
90
91
95
99
4.1
4.2
Introduction . . . . . . . . . . . . . . . . . . . . . . . . . . . . . . .
Dispersion model with tetrahedratic coupling (infinite pitch limit) .
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
4.2.1
4.2.2
4.2.3
Order parameters . . . . . .
Phases of model (4.1)	. . . Scope of presented research
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
4.3
Monte Carlo simulations . . .
.
.
.
.
.
.
.
.
.
4.3.1
4.3.2
4.3.3
Susceptibilities . . . .
Correlation functions .
Determining transition temperatures
4.4
4.5
4.6
Results for τ = 1 . . . . .
28
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
Results for τ =	. . . .
15
Discussion and summary .

Contents
xiii
5	Spatially modulated structures
101
. 101
. 102
. 104
. 105
. 105
. 108
. 110
5.1
5.2
Intermolecular vector coupling . . . . . . . . . .
Consequences of intermolecular vector coupling
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
5.2.1
One-dimensional chain .
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
.
5.3
Two-dimensional lattice . . . .
5.3.1
Simulations and results
5.4
5.5
Three-dimensional lattice	.
.
.
.
.
Discussion . . . . . . . .
.
.
6	Summary and conclusions
111
Bibliography
115

Chapter 1
Introduction
1.1
Liquid crystals, typical phases and symmetries
Liquid crystals are intermediate states of matter between liquids and crystalline solids,
possessing some of the properties of both. Anisotropic molecules, called mesogens, through mutual interaction produce macroscopic states which exhibit ordinary rheology like that of liquids, and macroscopic anisotropic properties observed in crystals, such as anisotropy of the dielectric polarizability, birefringence and Bragg peaks in X-ray and neutron scattering [2]. The liquid properties are due to the retained translational free- dom, while anisotropy is an effect of long-range orientational ordering of the mesogens, which on average align along macroscopic axes of anisotropy. Liquid crystalline states, called mesophases, occur in systems divided into two groups. In thermotropic liquid crys- tals phase transitions between mesophases occur with changing temperature (or altering the pressure). Several phases of different symmetry can be observed in sequence with decreasing temperature for the same compound, before it crystallizes to a solid. On the other hand, there are lyotropic liquid crystals, where the transitions occur with changing concentration of a component. They are, in general, mixtures of different compounds distributed in a solvent and the macroscopic ordering can be produced by alignment of individual molecules, but also of larger structures, such as anisotropic micellae [3, 4]. In the presented work we deal with thermotropic mesophases exclusively.
The initial discovery of a mesophase is attributed to botanist Friedrich Reinitzer, who
in 1888 noticed that the synthesized by himself cholesteryl benzoate exhibits two ther- motropic phase transitions in the liquid phase [5]. Subsequently, he performed several experiments involving polarized light, which revealed the anisotropic nature of the newly found state of matter. Puzzled by these discoveries, he contacted Otto Lehmann, who
1

Chapter 1. Introduction
2
initially asserted that the intermediate cloudy phase is in fact crystalline, but later con-
cluded that it is in fact an anisotropic liquid and continued Reinitzer’s research [6, 7]. Because the new phase bore the properties of both liquids and crystalline solids, the term “liquid crystal” was coined and is used to this day, generally in reference to compounds which produce mesophases. Liquid crystal research was not prominent for nearly half a century, but experienced an outburst after World War II, when in the oncoming decades followed many discoveries of new phases and successful theoretical descriptions [2–4, 8– 10] along with numerous practical and commercial applications, such as ubiquitous liquid crystal displays [11, 12] and electro-optical devices [13].
1.1.1
Typical thermotropic mesophases and symmetries
Thermotropic liquid crystal systems above the highest melting point (called the clearing
point) are ordinary liquids, characterized by the isotropic symmetry of the O(3) group of proper and improper rotations in 3D space. Lowering the temperature leads to a phase transition to a mesophase, in which directions of anisotropy are established by sponta- neous breakdown of rotational symmetry. The simplest example of mesophase, although not the first to be discovered, is the nematic phase. Calamitic (rod-like or cigar-shaped) mesogens with large longitudinal anisotropy (e.g. MBBA or PAA [2, c. 1.2]) possess (on average) an effective axis of cylindrical symmetry, while the intrinsic degrees of free- dom and anisotropy of secondary axes average out due to thermal fluctuations and the molecules align with their principal molecular axes in parallel. Among classical nemato- gens there are no known cases of compounds which produce stable polar nematic phases [14], hence the average alignment axis, called the director, has no preferred orientation. The (uniaxial) nematic phase has global symmetry of the D∞h point subgroup of O(3), which consists of continuous rotation about a fixed axis and one reflection plane perpen- dicular to the axis of symmetry. In this case, the global symmetry axis is the director. A phase of identical symmetry is also formed by discotic nematogens (e.g. hexasubstituted triphenylene [15]), which in average resemble flat disks. In this case the molecular axis of symmetry is perpendicular to the face of the disk, so that the macroscopic alignment of faces produces a uniaxial nematic phase. The two varieties are distinguished as uniaxial nematic prolate NU +, for the alignment of long molecular axes, and uniaxial nematic oblate NU −, for the alignment of faces.
Traditionally mentioned are also layered mesophases called smectics, in which there also occurs partial breaking of the translational symmetry and the distribution of centers of mass exhibits one-dimensional periodicity. Out of the vast variety of smectic phases, we name a few. The simplest smectic, known as smectic A (SmA), shows nematic order

Chapter 1. Introduction
3
a
b
c
d
Figure 1.1: Representations of common liquid crystalline phases: uniaxial nematic pro-
late (a), uniaxial nematic oblate (b), smectic A (c) and smectic C (d). The vector nˆ is the director.
(Qc Barrett Research Group, Creative Commons Attribution-Share Alike 3.0 Unported un- der fair use.)
within periodic layers with the director normal to the layer. In smectic C (SmC) the
director is tilted with respect to the layer normal by an angle.
1.1.2
Molecular chirality
The phenomenon of molecular chirality in mesogens leads to many new phases. Chiral
molecules are not symmetric with respect to a rotoreflection, just like one’s right hand cannot be rotated to match the left and vice-versa. Such molecules are optically active,
i.e. there is an asymmetry in the interaction of the molecule with the two helicities of light and the interaction can alter the light’s polarization [16]. Homogeneous macro- scopic chirality occurs when a compound, for various reasons, does not possess an isomer of opposite chirality or when the specific synthetization process favors one of them. The other case is that molecules of opposite handedness are equally abundant in a mixture. In this case, domains of opposite chirality can be formed. In terms of microscopic align- ment, molecular chirality leads to rotated ground states of two molecules with the same chirality, with a preferred helicity for two left-handed and two right-handed molecules. In homochiral samples or domains, this induces mesoscopic twisted states. Particularly, in chiral nematogens, in a homochiral domain there can exist a macroscopic wave vector along which the perpendicular director rotates, forming a helix with a helicity reflecting the handedness of the molecules. Cross sections perpendicular to the wave vector exhibit nematic ordering, while being rotated with respect to each other. This case describes the cholesteric phase, which was first found in cholesteryls (making it the first liquid crystal
phase discovered).
In some compounds the ground state is frustrated such that the energy minima with
respect to different directions cannot be achieved simultaneously and the frustration is relaxed by forming superstructures known as blue phases [17, 18]. Many chiral mesogens also form chiral layered phases, the simplest of which is the chiral smectic (SmC∗) phase,

Chapter 1. Introduction
4
a
b
Figure 1.2: Representations of common chiral liquid crystalline phases: cholesteric (a),
where the director nˆ is constrained to parallel, subsequently twisted planes, and chiral smectic (b), where the director nˆ is constrained to the surface of a cone and rotated between successive layers. (Qc Barrett Research Group, Creative Commons Attribution- Share Alike 3.0 Unported under fair use.)
in which the tilted director is subsequently rotated between neighboring layers (effectively
being constrained to the surface of a cone.)
1.2
Non-standard phases
While the uniaxial nematic has one axis of symmetry breaking (one Goldstone mode), in
a biaxial nematic the D∞h symmetry is further spontaneously broken and a secondary axis is formed. Because two distinct axes naturally distinguish a third one, normal to the plane of the first two, the resulting phase is expected to have anisotropic properties in three distinct directions. The symmetry of the biaxial nematic phase NB is of the point group D2h, the symmetry of a rectangular cuboid (Fig. 1.4a), which consists of reflections along three perpendicular mirror planes and three twofold symmetry axes perpendicular to the mirror planes.
By analogy, since uniaxial molecules produce the uniaxial nematic phase, the biaxial
phase should be formed by biaxial (brick-like or ellipsoloidal) molecules which align their primary and secondary axes in a long-range fashion. This was notably observed for anisotropic micellae in a lyotropic system by Yu and Saupe [19] and more recently in polymeric systems by Severing et al. [20], but the discovery of a thermotropic mesogen which produces the biaxial nematic phase has proved far more difficult. Intriguingly, most nematogens are intrinsically biaxial [21], but produce mostly stable uniaxial phases. The existence of the biaxial nematic phase has been subject to intensive studies [22–31].
Fairly new accounts report observation of the biaxial nematic phase in systems of bent-
core mesogens [27, 29], as predicted by Teixeira et al. [32], and tetrapode molecules [28]. The discoveries have been notably questioned [33] and alternative explanations of the results have been proposed [34], thus in the present there is no mutual consensus as

Chapter 1. Introduction
5
O
O
O
O
O
O
N
N
N
N
C 2 H 5 O
O C 2 H 5
Figure 1.3: An example of a bent-core molecule.
to the existence of the biaxial nematic phase, however the attention has been shifted to
non-standard mesogens, such as bent-core molecules and flexible dimers. The proposition that the biaxial nematic phase might be field-stabilized [34] motivates our work presented in chapter 3.
Bent-core mesogens are V-shaped molecules with a wide opening angle (typically 120 ∼
140◦) (e.g. see Fig. 1.3), which received interest after their synthetization by Matsunaga and Matsuzaki in the 1990’s [35]. In these systems several smectic phases have been discovered [36] and also complex supramolecular structures [37], some discoveries point to existence of chiral smectic layers [38–40], which is peculiar for achiral molecules. In general, bent or bendable mesogens in appear to exhibit chiral symmetry breaking and ambidextrous chirality (spontaneous formation of multiple domains of either handedness) through conformation changes or forming of superstructures [41], such as mesoscopic helical and heliconical shapes, as first predicted by Dozov [42] and evidenced by Monte Carlo simulations [40, 43]. Other examples include spontaneous breaking of chiral and tetrahedratic symmetry in some ferrocene mesogens, which are allowed to bend due to the cyclopentadiene rings’ freedom to rotate with respect to each other [44]. Recently, in flexible dimers (chainstick-like mesogens with a flexible separator, which can attain bent shapes and also are achiral) there have been reports of an entirely new phase, dubbed the twist-bend nematic phase [45–49], in which the molecules form heliconical structures of either handedness. As evidenced by freeze-fracture experiments by the group from University of Colorado in Boulder [50], these structures have pitch on the nanometer scale, spanning only several molecules, unlike in other chiral liquid crystals, such as the cholesteric, where the pitch of the helix is hundreds to thousands of molecules long. In some sense these discoveries violate the usual intuition that chirality is necessarily intrinsic. We explore the phenomenon of spontaneous breaking of chirality in chapters 4 and 5.
Symmetry considerations involving bent-core systems lead to a conclusion that a tetra-
hedratic order parameter should be included in their description [51, 52], which hints that phases of tetrahedratic symmetry may also be encountered. There are indications that this is indeed the case [53], furthermore it appears possible to induce tetrahedratic order by an external field in bent-core systems [54, 55]. The tetrahedratic phase T is optically isotropic (easily mistaken for the isotropic phase) and has the global symmetry

Chapter 1. Introduction
6
a
b
Figure 1.4: a) A rectangular cuboid – object possessing the symmetry of the point group
D2h.
b) A regular tetrahedron – object possessing the symmetry of the point group Td.
of the point group Td, which is the symmetry group of the achiral regular tetrahedron
(Fig. 1.4b). An achiral regular tetrahedron has four threefold axes, which pass through its vertices and the center, and three twofold axes, which lie on the midpoints of opposing edges. There are six mirror planes formed by two threefold axes and six mirror reflections combined with a rotation by 90◦. Together with the identity Td is of the order 24. The
inclusion of tetrahedratic symmetry is discussed in chapter 4.
1.3
Introduction to order parameters in liquid crystals
The long history of active liquid crystal research has driven the development of a vast
multitude of theoretical and computational approaches to the subject, much of which were applied from theories of phase transitions existing in statistical physics. While the interactions between mesogens are quite complex and calculating their approximations has grown into separate fields of research, much of this intrinsic complexity can be sacri- ficed when one isolates the crucial properties of the considered molecules. For instance, in uniaxial nematics it is sufficient to consider a unit vector cˆi, parametrized accordingly, to describe the orientation of the i-th molecule. (We remember that the translational de- grees of freedom are free and at this point we do not need their explicit parametrization.) The normalized ensemble average
 cˆi)
= nˆ,
(1.1)
| cˆ)|
is called the director and represents the average direction of long-range ordering of the
molecules in the sample. An appropriate order parameter which takes into account how well, on average, the molecules are aligned with the director is defined as (see e.g. [2]):
1
S =	3cos2θi − 1),
(1.2)
2

Chapter 1. Introduction
7
which is the ensemble average of the second Legendre polynomial P2(cosθi). One should
notice that since the molecule (on average) looks the same when reflected along cˆi, the vector −cˆi is an equally good representation of the orientation of molecule i, thus a choice of cˆi · _n) = cosθi) is not a proper order parameter, as it averages to zero, due to lack of long range polar order.
A thermotropic nematic above the clearing temperature forms an optically isotropic
liquid, i.e. a phase of uniform spherical symmetry of the rotation group O(3). In such phase there is no preferred direction and therefore nˆ is not a well-defined vector. The symmetry enables us to choose any frame of reference, and the average (1.2) yields zero. When the clearing point is approached with lowering temperature, the vector nˆ is established by spontaneous symmetry breaking. If one knows _ci, i = 1, 2, · · · , N , the instantaneous director and S can be computed. S becomes non-zero (in fact abruptly for uniaxial nematics) and continues to rise as the temperature is lowered. In real systems we eventually reach another phase transition, e.g. to a smectic phase or crystalline solid, depending on compound. In an abstract sense, S would reach one if the molecules aligned precisely along the director. In experiment, S can be measured directly by e.g. NMR, birefringence or Raman scattering [2].
Calculating order parameters like (1.2) involves computing non-trivial integrals.
general microscopic property A:
For a
I
l
ˆ
ˆ
 A) = Z−1 Tr	A({Ω , η })e
−βH({Ω ,r })
i i
,
(1.3)
i	i
{Ωˆ i,ri}
Ie−βH({Ωˆ i,ri})l ,
Z =	Tr
{Ωˆ i,ri}
(1.4)
where β = (kBT )−1 and H({Ωi, ri}) is the Hamiltonian of the system, which depends
on the considered model (e.g. the Maier-Saupe Hamiltonian (1.8), discussed later). In the above, we have assumed that the kinetic part can be integrated separately. Thus, the trace is performed over the remaining rotational and translational ri degrees of freedom. In the case of rotational degrees of freedom, the trace is understood as SO(3)-invariant integration, therefore calculating (1.3) amounts to evaluating two 3N - dimensional integrals. Mean-field theory (section 1.7) and Markov chain Monte Carlo (section 1.8) provide methods for approximating (1.3), allowing one to escape the infea- sibility of calculating such a large-dimensional integral.
Ωˆ i

Chapter 1. Introduction
8
1.4
Dispersion forces
The dispersion interaction, known in chemical literature as the London dispersion forces,
first described by Fritz London (1900-1954) [56], is a type of Van der Waals interaction encountered in the second order of the quantum perturbation theory of interaction be- tween two molecules at a large distance R_ 12 [57]. The long-range character allows one to treat the interaction as a perturbation to the Hamiltonian of the free particle. The per- turbative contribution to the energy of the pair ground state from dispersion interactions reads [58]:
(1) (2)
(1) (2)
2
)
1
 ψ0 ψ0 |Hl|ψr ψs
\

r/=0,s/=0
udisp. = − 2
(2) ,
(1.5)
W (1)
(1)
(2)
— W0	+ Ws	− W0
r
where ψ(k) is the ground state of k-th molecule, while ψ(k) are its excited states.
W (k)
q
0
0
and W (k) are energies of the corresponding state. The perturbation Hl is simply the net
q
electrostatic potential of interaction between all the charges residing at both molecules:
(1) (2)
1 \ ei
ej
Hl =
.
(1.6)
2
rij
ij
Subsequently, Hl can be expanded in a multipole series and following premises depending
on the considered molecules, some terms are discarded, others treated as dominating. Note that in the above expression both molecules are in excited states. Intuitively, the interactions are due to the fact that thermal fluctuations of the charge distribution on one molecule result in a momentary excited multipolar state (dipole, quadrupole, octupole, etc.) which in turn induces an excited multipolar moment on the other molecule. Hence, the contribution is due to coupling between induced multipoles.
In nematogens, which are mostly large, organic molecules, the dispersion term dominates
over other electrodynamic effects because it is proportional to the volume of the molecule. Other important contributions include electrostatic interactions due to static multipoles, such an electric dipole in bent-core molecules (see e.g. [36]). The dispersion interaction is easier to account for in calculations than purely electrostatic forces because of its effectively short range. In many cases the interaction can be constrained to the nearest neighbors without much sacrifice. However, it should be noted that the main cause for nematic ordering is excluded-volume (steric) effects, although the leading terms, in most cases, turn out to be similar to the leading dispersion terms. For example, dispersion and steric terms alike, in the case of the uniaxial, nematic yield interaction proportional to the second Legendre polynomial in the cosine of the intermolecular angle, as considered for dispersion interaction by Maier and Saupe [59–61] and as found by Onsager for the steric case [62]. Excluded volume effects produce phase transitions where the analogue of

Chapter 1. Introduction
9
1 .
temperature is the inverse concentration	To account for the temperature dependence
ρ
of the order parameters, thermotropic nematogens are studied mainly by dispersion-like models. For notable examples, dispersion interactions have been considered for uniaxial nematics by Maier and Saupe [59–61] (see also subsection 1.5.1), for biaxial nematics by Luckhurst et al. [63, 64], and for chiral symmetry breaking in bent-core molecules by
Longa, Pająk and Wydro [1]. We will return to the last two models in chapters 3 and 4.
1.5	Historical results
1.5.1
Maier-Saupe model of thermotropic nematics (lattice case)
An important result in the context of the presented work is the one of Maier and Saupe
presented in a series of papers in 1958-1960 [59–61]. It is a specific application of the mean-field method, which we present in section 1.7, to a microscopic model of a uniaxial nematic, which allows for describing the thermotropic nematic phase transition. Maier and Saupe’s basic assumption was that the pair interaction potential between molecules i and j is due to point dispersion forces. The pair interaction potential is expanded in a multipole series in the the representation of spherical harmonics. By request, only uniaxially symmetric terms, i.e. with m = 0, enter the expansion, which makes it sufficient to consider an expansion in Legendre polynomials. Therefore one obtains:
α2
V (rij, θij ) = − r6 [P2(cosθij ) + . . . ] ,
(1.7)
ij
where rij is the relative distance between molecules i and j and θij is the relative angle
between axes _ci and _cj (as in Fig. 1.5). P1 and other odd terms are dropped since the interaction should be symmetric with respect to _ci(j) → −_ci(j), as polar ordering is being neglected. In the general case the mean-field calculation involves an approximation of the
two-point spatial correlation function by a step function, which is zero for	∈ [0, r0)
rij
Figure 1.5: Two molecules with their orientations described by vectors _ci and _cj . The
intermolecular angle can be expressed as cos θij = _ci · _cj .

Chapter 1. Introduction
10
and constant otherwise, to model the hard-core repulsion between molecules at close
distances smaller than r0. However, if the molecules occupy sites of a simple cubic
lattice and interact only with their nearest neighbors, one can put	= a in (1.7), a
being the lattice constant, thus lifting the need to integrate over positional coordinates. Neglecting higher-order terms, while taking α2/a6 ≡ α0, one arrives at:
rij
V (cosθij ) = −α0P2(cosθij ),
1 \
(1.8)
H =
 ij)V (cosθij ),
2
which represents the Maier-Saupe l = 2 minimal coupling model on the lattice. If we
β−1
define the dimensionless temperature as t =
potential reads:
= kBT/α0 (see e.g. (3.1)), the pair
1
2
V (cosθij ) = −P2(cosθij ) = − 2 (3cos θij − 1).
(1.9)
Now assume that the system can be described by the single-particle distribution function
f (θ) for the orientation of molecules with respect to the director. This allows one to write a single-particle average of the pair interaction potential, called the effective potential:
r
Vef (cosθi) =	dθjf (θj )V (cosθij ).
(1.10)
Furthermore, f is expanded similarly as V in terms of Legendre polynomials:
∞
f (cosθk ) = f (_ck · _n) = \ Pl)Pl(_ck · _n),
l=0
(1.11)
where k numbers an arbitrary particle. Substituting (1.9) and (1.11) into (1.10):
r
∞
Vef (cosθi) = Vef (_ci · _n) = −	dθj \ Pl)P2(_ci · _cj )Pl(_ck · _n)
l=0
(1.12)
and observing the orthogonality laws of Legendre polynomials, we arrive at:
Vef (cosθi) = − Pl)P2(_ci · _n) = − Pl)P2(cosθi).
(1.13)
In mean-field theory, (1.13) is used to construct the so-called equilibrium
single-particle distribution, which can be used to calculate averages:
mean-field
Peq (cosθ) = Z−1exp(−βVeff (cosθ)),
r
Z =	dθexp(−βVeff (cosθ)),
r
 P2) =	dθP2(cosθ)Peq (cosθ).
(1.14)
(1.15)
(1.16)

Chapter 1. Introduction
11
Because P2) appears in (1.14) and (1.15), this set of
equations is self consistent. We
recognize that P2) is precisely the parameter S as defined in (1.2). For the sake of brevity
we only indicate that these equations can be solved by numerical methods. The phase transition is of first order at Tc ≈ 0.22 with a sudden jump of S from 0 to S(Tc) ≈ 0.44.
1.5.2
Lebwohl-Lasher lattice model
The model of central importance as background to the presented work is the Lebwohl-
Lasher lattice model of the uniaxial nematic. In 1972 Lebwohl and Lasher performed pioneering Monte Carlo simulations of a nematic in a lattice setup [65]. The setup consisted of molecules placed in the nodes of a 3-dimensional simple cubic lattice, with interactions restricted to the nearest neighbors and periodic boundary conditions, while the pair potential was adapted from (1.9):
Vij = −EP2(cosθij ),
1 \
(1.17)
H =
Vij.
2
(i,j)
The summation runs over nearest neighbors on the lattice, i.e. for each i summation over
j runs over six neighboring particles. The authors considered 10 × 10 × 10 lattices far from the transition and 20 × 20 × 20 in the transition vicinity and considered sample sizes between 2000 and 8000 to discover a discontinuity of the mean energy, indicating a first- order phase transition at E/kBT = 0.850 ± 0.005 with a jump of the order parameter S of
∆S = 0.33 ± 0.04. The results have been subsequently refined by Fabbrio and Zannoni for 30 × 30 × 30 lattices, who observed the phase transition at E/kBT = 0.8903 ± 0.0005 [66]. Due to its simplicity and practical significance, Lebwohl and Lasher’s approach is
often treated as a template in performing simulations of bulk liquid crystals.
1.6	Alignment tensor
In the general case, where apart from uniaxial ordering along director nˆ, the phase
exhibits biaxial ordering (and two secondary biaxial directors {l, mˆ } are established), it is concisely described by one tensorial parameter, called the alignment tensor:
ˆ
1
Q = S(_n ⊗ _n − 3 I) + T (_l ⊗ _l − m_ ⊗ m_ ).
(1.18)

Chapter 1. Introduction
12
Here S is the familiar uniaxial parameter, as defined in (1.2), while T is the biaxial order
parameter. According to a definition by Straley [67]:
T = sin2(θ)cos(2φ)),
(1.19)
where {φ, θ} are two of the three Euler angles, defined by consecutive rotations:
Rz (φ)Ry (θ)Rz (ψ). One recognizes that the function being averaged on the right-hand side of (1.19) is (up to a normalization constant) the real part of the spherical har-
monic Y l (θ, φ) for l = 2, m = 2, Y 2(θ, φ). As we later discuss, in general the l = 2
m
2
representation of SO(3) proves very useful in the context of biaxiality.
_
The tensor (1.18) is traceless, symmetric and diagonal in the director basis {l, m_ , _n},
where it reads:


S
− 3 + T
0
0
0
0
0
Q = 
 .
S
(1.20)
—	− T


3


2 S
0
Q can be
3
inferred. For instance, if S /= 0
From the above form a few properties of
_
and T = 0, i.e. in the uniaxial nematic phase, Q is degenerate in the {l, m_ } plane,
while the non-degenerate eigenvalue corresponds to the uniaxial director _n. Conversely, in the biaxial phase T /= 0 and all the eigenvalues are different. Because the tensor is traceless by definition, in the isotropic phase it equals to zero. Furthermore, the sign of the largest-modulus eigenvalue of Q informs us whether the uniaxiality is of the prolate (rodlike) (+) or oblate (discotic) (−) variety.
It is often more practical to deal with Q directly than with S and T , as in phenomeno- logical Oseen-Frank [68, 69] or Landau-de Gennes [2] theories. For instance, in the latter case, Q enters the expansion of the Landau free energy in the form of absolute rotational invariants Tr(Q2) and Tr(Q3). As it turns out, these are the only invariants without involving derivatives of Q, as from matrix algebra it follows that all invariants of higher order can be expressed by Tr(Q2) and Tr(Q3) [70]. These invariants hold a relation:
Tr(Q3)2 ≤ 1 Tr(Q2)3 [70], which can be expressed with one condition	≤ 1 [71, 72],
w2
6
where:

3
Tr(Q )
w = √6
.
(1.21)
(Tr(Q2))3/2
For the uniaxial case w = ±1 and the sign distinguishes the prolate (+) and oblate (−)
varieties. For the biaxial phase w2 < 1, while the case w = 0 corresponds to the case of “maximum biaxiality”, when the eigenvalues of Q are {ω, 0, −ω} (in any order).

Chapter 1. Introduction
13
1.7
Mean-field theory for lattice models
As argued in section 1.3, an exact evaluation of the statistical average (1.3) is impractical
in macroscopic systems. We present the mean-field method of producing an approxi- mation for the equilibrium particle distribution, where the total number of degrees of freedom in the ensemble average is reduced by a factor of N . First, let us recall from statistical mechanics that the equilibrium state of the system in the canonical ensemble is given by minimum of the inequilibrium Helmholtz free energy functional [73, 74]:
Fneq [P ] = U [P ] − TS [P ] ,
(1.22)
where P = P (x1, x2, x3, · · · , xN ) is the N -particle probability of finding the system in
the state such that particle 1 is in the state x1, particle 2 is in the state x2, etc. We assume that the translational degrees of freedom are fixed and the N molecules reside on lattice sites, therefore the state xi of the i-th particle is parametrized by its orientation
Ωˆ i (xi ≡ Ωˆ i). A trace over all possible states, Tr , is therefore understood as an SO(3)-
{Ωˆ i}
invariant integral over Ωˆ i (e.g. for the parametrization of Ωˆ i by Euler angles {αi, βi, γi}, such that the rotation matrix carrying from the laboratory reference frame to	is
R(Ωˆ i) = Rzˆ(γ)Ryˆ(β)Rzˆ(α), where Ri(η) is a proper rotation about an angle η around
Ωˆ i
axis i, the trace reads Tr ≡	[ 2π dα [ π sinβdβ [ 2π dγ). At this point we assume that
1
8π2 0
0
0
{Ωˆ i}
no continuous conformational degrees of freedom are present. If discrete conformational
degrees of freedom are to be included, the trace needs to be supplemented by a sum
over discrete conformational states. (An example is the chirality degree
introduced in section 4.2.) The equilibrium free energy is given by:
of
freedom,
Feq = Fneq [Peq ] ,
(1.23)
where Peq satisfies the conditional minimum equation:
(
(

δ
δP l
Fneq [P ] − λ	Tr P (Ωˆ 1 · · · Ωˆ N ) − 1	= 0.
(1.24)
{Ωˆ i}
We account for the constraint that P should be normalized through the Lagrange mul-
tiplier λ. (1.22) can be written explicitly using Shannon entropy:
Fneq [P ] = Tr IH(Ωˆ 1 · · · Ωˆ N )P (Ωˆ 1 · · · Ωˆ N )l + kBT Tr IP (Ωˆ 1 · · · Ωˆ N )logP (Ωˆ 1 · · · Ωˆ N )l .
{Ωˆ i}
{Ωˆ i}
(1.25)
Integration over momenta is not taken into account, as for the models we are going
to consider the kinetic part of the Hamiltonian gives an additive constant to the free energy. Generally, we assume that the Hamiltonian is a sum of pair interactions and

Chapter 1. Introduction
14
single-particle potential energy (e.g. interaction with external field):
N
N
V (Ωˆ i, Ωˆ j ) −	V (Ωˆ i).
i
1
 \
2
\
H(Ωˆ 1 · · · Ωˆ N ) =
(1.26)
(i,j)
Summation over i, j) means that nearest-neighbor interaction is assumed, i.e. that each
molecule i interacts only with its z neighbors. z is the coordination number, which depends on the lattice structure (e.g. z = 6 for a simple cubic lattice with periodic boundary conditions).
The main assumption of the mean-field approximation is that P (Ωˆ 1, Ωˆ 2, · · · , Ωˆ N ) factor- izes into identical single-particle distribution functions P (Ωˆ ):
P (Ωˆ 1, Ωˆ 2, · · · , Ωˆ N ) = P (Ωˆ 1) · P (Ωˆ 2) · · · · · P (Ωˆ N ).
(1.27)
With this assumption, (1.25) reduces to:
N
\
1
I
l
ˆ	ˆ	ˆ	ˆ
Fneq [P ] = 2
Tr	P (Ωi)V (Ωi, Ωj )P (Ωj )
ˆ ˆ
(i,j) {Ωi,Ωj }
(1.28)
N
\

i
N
I
l
I
l
\
Tr	P (Ωˆ i)V (Ωˆ i) + kBT	Tr	P (Ωˆ i)logP (Ωˆ i) .
−
{Ωˆ i}
{Ωˆ i}
i
Now solving the minimum condition (1.24) is a matter of applying the rules of functional
calculus and algebra. The Lagrange multiplier λ is calculated from the normalization condition. The resulting equilibrium particle distribution function reads:
ˆ	ˆ
ˆ
−1 −β(V
(Ω)+V (Ω))
P (Ω) = Z	e
eff
,
(1.29)
eq
eq
I
l
ˆ	ˆ
−β(V
(Ω)+V (Ω))
Zeq = Tr e
{Ωˆ }
eff
,
(1.30)
where the “effective potential” is defined as:
z
Veff (Ωˆ j ) = \ Tr IPeq (Ωˆ i)V (Ωˆ i, Ωˆ j )l .
(1.31)
ˆ
i/=j {Ωi}
Furthermore,
1
I
l
Feq = − 2 N Tr Peq (Ωˆ )Veff (Ωˆ ) − NkBTlogZeq.
(1.32)
{Ωˆ }
The interpretation of (1.31) is that instead of involving the interactions of particle j with
every of the other N − 1 particles explicitly, we treat j as if it were immersed in a field (Veff ) of interactions averaged over all the other particles, hence the term “mean-field”

Chapter 1. Introduction
15
theory. The equations (1.29-1.31) are self-consistent, i.e. one generally cannot write a
solution in closed form and they should be treated by e.g. iteration to convergence.
The mean-field approach has the advantage of being relatively simple and computation-
ally inexpensive. However, the transition temperatures are overestimated with respect to experiment and simulations, due to the assumption (1.27), i.e. that many-particle correlations are neglected. Because of this, entropy is underestimated, which enables the potential energy to dominate to higher temperatures than in reality. Another prop- erty of mean-field theory is that it produces Landau critical exponents regardless of the Hamiltonian in question (and therefore its applicability in studying critical behavior is limited).
1.8	Monte Carlo simulations
1.8.1
Metropolis algorithm
To calculate the average (1.3), we also use the Markov chain Monte Carlo method, which
in the modern version was described by Stanisław Ulam and Nicholas Metropolis in the 1940’s [75]. The name, owing to Ulam, is purportedly derived from the Monte Carlo casinos, in a reference of the method to gambling. The basics of the method stem from the Central Limit Theorem and sampling the equilibrium probability distribution by generating a Markov chain.
The Central Limit Theorem, applied to the canonical ensemble,
dimensional integral:
states
that
the n-
r
 A) =	dx1 · · · dxnA(x1, · · · , xn)
e−βH(x1,...,xn)
(1.33)
Z
can be replaced by an average over N samples {xi}:
1
N
\

{xi}:p({xi})
N →∞
 A) →
A(x1, · · · , xn),
(1.34)
where the samples {xi} are drawn from:
p({xi}) = Z−1e−βH(x1,...,xn).
(1.35)
An algorithm which allows sampling of p({xi}) is given by Metropolis [76]. The pre-
scription amounts to designing an ergodic Markov process that asymptotically reaches

Chapter 1. Introduction
16
p({xi}) as the stationary distribution. This is done by observing that such a process
needs to conform to detailed balance:
p({xi})σ({xi} → {xj }) = σ({xj })p({xj } → {xi}),
(1.36)
where σ({xi} → {xj }) is the probability of transition of the system from
state i to j.
Detailed balance secures that the transition is reversible, i.e. that the considered system
is in equilibrium. The equilibrium probability distribution is given by (1.35), so rewriting (1.36):
e−βH({xi})
p({xi} → {xj })
p({xj } → {xi})
= e−β∆Eij ,
=
(1.37)
e−βH({xj })
where ∆Eij is the difference of energy between the two equilibrium states. The pre-
scription due to Metropolis is that we can achieve the relative probability (1.37) in a simulation of the system by following an algorithm:
1.
Starting with the system in the state i, make a small random change in i, thus
creating the “trial” state j and calculate the energy difference ∆Eij .
2.
If ∆Eij ≤ 0, accept j as the new state of the system unconditionally.
If ∆Eij > 0, accept j as the new state of the system with the probability e−β∆Eij .
3.
4.
Repeat 1-3 for a suitable sample size.
This
algorithm produces a random walk in the state space of the system. For a good
convergence to the real distribution p({xi}), the space of equilibrium states needs to be
explored quite extensively. The question is how large the change to i in pt. 1, i.e. the random-walk step should be. Very large changes will almost never be accepted, while very small ones will have the system stuck in one area of the state space for a very long time. Generally, a rule of thumb is assumed that the step should be of such magnitude, that the fraction of accepted moves is around 0.4 ÷ 0.5. In most cases the changes will be small enough so that states i and j will be substantially correlated, thus making the random walk non-Markovian. To obtain a good Markov chain, one needs to discard a number of intermediate states until no correlation is measured. The final result is a Monte Carlo sample of the statistical ensemble, i.e. a set of replicas of the system in equilibrium. On the other hand, ergodicity permits us to regard the replicas as snapshots of a single system undergoing an equilibrium process.
There remains the problem of the choice of the initial state i, since an arbitrary state
will likely be out of equilibrium. While the Metropolis algorithm is designed to produce an approximation for the equilibrium distribution function, it can be used to find an

Chapter 1. Introduction
17
equilibrium process through random walk in state space, which drifts towards an energy
minimum, in a non-equilibrium process called thermalization. Once thermalization is complete, sampling of equilibrium states can begin. A question open to the scientist is to make sure that the system is not stuck in a metastable state.
1.8.2
Rotational degrees of freedom
In the presented work the simulations are performed in the spirit of Lebwohl and Lasher
(see section 1.5.2), i.e. the Monte Carlo degrees of freedom are limited to the orientation of molecules (in later chapters we also consider chirality). There are several parametriza- tions of rotations in 3D space, e.g. Euler angles, which describe the subsequent rotations of the frame of reference around axes zˆ,xˆ and zˆ. The computational disadvantage of this and many other methods is the need of evaluating trigonometric functions. In Monte Carlo simulations such evaluations are performed for each particle in each attempted move, which can turn out to be substantially expensive. For this reason we parametrize rotations using quaternions, which reduces the problem to evaluating second-order poly- nomials [77].
The parametrization follows from the fact that the group SU (2) of unitary 2 × 2 matrices
of determinant 1:
(

u1	u2
U =
,
(1.38)
−u∗
u∗
2	1
U † = U −1,
(1.39)
2
2
detU = |u | + |u |
= 1,
(1.40)
1
2
is a double universal cover of SO(3), the group of 3×3 orthogonal matrices of determinant
1. On the other hand, SU (2) is isomorphic with the group of quaternions with norm 1:
(

q0 + iq3	iq1 − q2
iq1 + q2	q0 − iq3
U =
,
(1.41)
q = q0 + q1i + q2j + q3k,
(1.42)
|q|2 = detU = q2 + q2 + q2 + q2 = 1,
(1.43)
0	1	2	3
where q is a quaternion. Thus, the space of rotations in 3D space is replaced by a set of
points on the unit 4D sphere. The mapping is given by expressing the rotation matrix

Chapter 1. Introduction
18
in terms of q (see e.g. [77]):


q2	2	2	2
0 + q1 − q2 − q3
2(q2q1 + q0q3) 2(q3q1 − q0q2)
2(q1q2 − q0q3)
2(q1q3 + q0q2)
2(q2q3 − q0q1)
R = 
 .
2
2
2
2
3
(1.44)
q − q + q − q


0
1
2


2
2
2
2
3
2(q3q2 + q0q1)
q − q − q + q
0
1
2
Note that R does not change if q → −q, which reflects the fact of double covering. The
matrix (1.44) gives us the reference frame rotated according to q. As stated before, when comparing the rotation matrix for Euler angles and (1.44), it is readily seen that the quaternion version is computationally cheaper to evaluate.
To make use of quaternions in Monte Carlo, we need a means of generating random
rotations expressed in quaternions. The parametrization (1.41-1.44) simplifies this task by reducing it to drawing points from an uniform distribution on a 4-sphere, because the invariant measure for SU (2)-invariant integration is uniform for quaternions, i.e.
[
2
2
Tr ≡	δ(q + · · · + q − 1)dq . . . dq for the canonical ensemble average (1.3). The
0
3
0
3
{Ωˆ i}
algorithm used in the presented work is due to Marsaglia [78].
independent points from the unit circle:
First,
we
draw two
p1 = (y1, y2), p2 = (y3, y4), yi ∈ [−1, 1],
(1.45)
r2	2	2
1 = y1 + y2 ≤ 1,
(1.46)
r2	2	2
2 = y3 + y4 ≤ 1.
(1.47)
If so, the point:
I
I
(y1, y2, y3	(1 − r2)/r2, y4	(1 − r2)/r2)
(1.48)
1	2
1	2
is uniformly distributed on the unit 4-sphere. Thus, we simply need to draw a quaternion
with accordance to (1.48) to produce a random rotation in 3D space.
However, if one makes a trial move on a molecule by simply replacing the quaternion
describing its rotation by a new, random one, the relative change will be most likely quite large and many moves will be rejected. Therefore, we perform the trial move by slightly altering the present orientation of the molecule. Considering that q is the quaternion for the molecule in question, we draw a random quaternion ∆q according to (1.48). Then, the new quaternion ql is:
q + r∆q
ql =
,
(1.49)
|q + r∆q|
where 0 < r ≤ 1. The parameter r can be adjusted to ensure proper acceptance ratio
of trial Monte Carlo moves. To calculate the difference in energy, one can rewrite the Hamiltonian using quaternions and do away with (1.44) completely during the calcula- tion. We, however, found that (1.44) bears an infinitesimal cost worth the advantage of

Chapter 1. Introduction
19
Figure 1.6:	A simplified, 2D illustration of how a Monte Carlo trial orientation (parametrized by quaternion ql) is constructed as a small deviation from the previous
orientation (parametrized by quaternion q), with the prescription (1.49).
retaining the original expression in terms of e.g. Cartesian tensors built on the molecular
basis {eˆx, eˆy , eˆz } given by R.
1.8.3
Parallel sampling and pseudorandom number generation
Once we have an equilibrium state at our disposal, we can take advantage of parallel
computing to either increase the sample size or reduce the time needed for the simulation to complete. This is performed formally by branching the random walk in state space into k random walks, which can explore the state space independently. If the random walks are non-correlated, the generated sets of equilibrium states can be treated as one sample of the statistical ensemble. Computationally, this is performed by first thermalizing the system into equilibrium and then taking k replicas, which are considered as initial states of k independent Monte Carlo simulations in separate threads. The results are aggregated at the end.
The principal problem of this method is ensuring that the resulting Markov chains are
non-correlated, which amounts to securing that each of the threads has its own, unique sequence of pseudorandom numbers. This issue is studied extensively and has been addressed recently for the Mersenne Twister algorithm on graphic processors by Pod- lozhnyuk [79] and earlier for linear congruential generators by Durst [80]. A method involving cellular automata has been proposed by Hortensius et al. in 1989 [81]. In the presented work we use a relatively new pseudorandom number generator family in- vented by Marsaglia in 1994 [82, 83] popularly referred to as “multiply-with-carry”. The sequence of the generator is defined as:
xn+1 = (axn + cn) mod b
(1.50)

Chapter 1. Introduction
20
where a is a multiplier and b is a modulus, which is typically 232 for 32-bit and 264 for
64-bit processor architectures. cn is the carry, defined as:
axn−1 + cn−1 b
cn = l
(1.51)
J
The multiplier a needs to be chosen such that ab − 1 is a safe prime, i.e. both ab − 1
and (ab − 1)/2 − 1 are prime. The period of (1.50) is of the order of b, thus greatly improved by utilizing the 64-bit architecture. The advantage of (1.50) is that one can produce infinitely many generators for a given b. Thus, at the expense of a small period,
219937 − 1,
when compared to e.g. that of Mersenne Twister, equal to
we can generate
non-correlated sequences of pseudorandom numbers by specifying different multipliers
and seeds to separate threads, instead of sharing one generator, which comes with im-
232
plementation issues. In our software, we use the multipliers and seeds for modulus
generated by Gratton [84].
1.9
Purpose and plan of thesis
The aim of the present thesis is to study some of the remarkable effects observed in
systems such as bent-core and ferrocene mesogens, as well as flexible dimers, including field-stabilized biaxiality, homogeneous chirality and twisted states of homogeneous and ambidextrous chirality, through a lattice dispersion model with the help of the meth- ods cited in this chapter – primarily by Monte Carlo simulation and, to a lesser extent, mean-field theory. The dispersion model being studied is an extension on models pre- viously considered in literature, of which all are generalizations of the Lebwohl-Lasher lattice model, discussed in section 1.5.2. The definition of this general model, along with descriptions of the respective terms and their purposes is given in Chapter 2, after a brief introduction to the formalism of irreducible tensors and symmetrization. Since this model is quite broad in scope and embraces six independent parameters, our aim is constrained to investigating several limit cases of the general model.
In Chapter 3 the case of a dispersion model of biaxial nematics in an external field
is considered. The interaction potential (3.14) is based upon the model by Luckhurst and Romano [64], augmented by a term which is quadratic in field (see (3.12)). The field considered is a generalized vector field, thus the effects apply (almost) equally to the magnetic and electric cases. The field-interaction potential promotes alignment of either the molecular axis of largest anisotropy or the largest molecular face, depending on the sign of the anisotropy of the generalized (dielectric or diamagnetic) molecular polarizability. Furthermore, the Luckhurst-Romano model, expressed in (3.1), introduces
a parameter for controlling the biaxiality of molecules, λ, which ranges from 0 to ;3/2.

Chapter 1. Introduction
21
1
The values
correspond to prolate (rodlike) and oblate (discotic) shapes for λ <
√6
1
1
and λ >
respectively, while λ =	is a highly-symmetric value, for which the model
√6
√6
exhibits a direct phase transition from the isotropic phase to a biaxial phase of maximum
biaxiality. Therefore, we study the model with external field considering different values
1
of λ (λ = 0.3, λ = 0.5 and λ =	) and the sign of the anisotropy of the molecular
√6
polarizability (positive and negative), while observing the effects of varying magnitude
of the external field.
The liquid crystalline phases originally known to exist for the Luckhurst-Romano model,
presented in the phase diagram in Fig. 3.3, are the isotropic (I), uniaxial nematic prolate and oblate (NU + and NU −) and biaxial nematic (NB ). After an introduction of order parameters and the details of the theoretical methods used (section 3.4), as a test of out methods we present results for this model in section 3.5. In section 3.6 we proceed to presentation of results for the model with external field, starting with an analysis of the critical and tricritical points of the isotropic-uniaxial nematic transition in section 3.6.1. We then move on to the Monte Carlo results, compared with mean-field predictions, for λ = 0.3, for which value the mean-field phase diagram in the (t, ∆Eh2)-plane (t being the dimensionless temperature and h being the magnitude of the field) is compared with the energy fluctuation landscape obtained from simulation, in section 3.6.2. For λ = 0.5 the mean-field phase diagram is obtained, presented in section 3.6.3. For the highly-
1
symmetric value of λ =	the mean-field phase diagram is obtained and supplemented
√6
by temperature scans of the order parameters, fluctuation of energy and susceptibilities
of order parameters in section 3.6.4.
In Chapter 4 the case of the biaxial nematic model with added tetrahedratic coupling
(without the presence of a field) is investigated. The interaction potential, first postulated in [1], consists of the quadrupolar coupling term, as in the Luckhurst-Romano model, and an octupolar coupling term, scaled by the coupling constant κ. The relationship between the D2h symmetry of the molecular quadrupolar moment and the Td symmetry of the molecular octupolar moment produces two possible chiral molecular configurations, distinguished by the parity of the molecular basis, which is considered as a binary degree
28
of freedom. We study this model for τ = 1 and a highly-symmetric value τ =	with
15
Monte Carlo simulations. For both cases there exist phases of tetrahedratic and chiral symmetry, while for the latter case a direct transition from the isotropic to the chiral
phase exists. The results are presented in sections 4.4 and 4.5 respectively.
The results contained in Chapter 5 are meant to be approached as preliminary. In
this chapter we consider the model studied in Chapter 4 with an added term, which accounts for coupling of the molecular octupolar moment to the intermolecular lattice vectors. As argued in section 5.2, this kind of coupling produces twists between molecules

Chapter 1. Introduction
22
on neighboring sites, as is promptly demonstrated in
simulation on a one-dimensional
chain. Subsequently, a two-dimensional case is considered in section 5.3, for which the
chiral-symmetry-breaking phase transition is studied and two types of structures in the chiral phase are identified. The three-dimensional case is discussed in section 5.4 and as of the moment of completion of this thesis the results presented are still largely open to interpretation. Two types of structures are found and presented in Fig. 5.6. Words of conclusion and comment on further studies are found in the closing Chapter 6.

Chapter 2
Generalized dispersion model for
bent-core (and related) systems
Before we define the model studied here itself, we first provide an introduction to the tool
which is central to the understanding and formulation of the former – the formalism of symmetrized irreducible spherical tensors. An explicit definition of the model in question is given subsequently in section 2.2.
2.1
Irreducible tensors and symmetrization
From the argument in section 1.4 it follows that dispersion interactions amount to cou-
pling of multipolar moments, which can be expressed in terms of Cartesian tensors. For dispersion models which possess global rotational symmetry this representation is how- ever often unoptimal. A more practical approach is to express the tensors involved in the dispersion interaction in terms of spherical tensors, which obey much simpler transfor- mation laws when undergoing rotations, i.e. they are always confined to the same fixed-l subspace of angular momentum [85].
Irreducible spherical tensors of rank n (the number of Cartesian indices), for angular
momentum quantum number l (l = 0, 1, · · · , n − 1, n) and projection of angular momen- tum quantum number m (m = −l, −l + 1, · · · , l − 1, l) are denoted as eˆm . They can be expressed within an ordinary Cartesian basis {eˆx, eˆy , eˆz }, which can be later on identified with the molecular basis or the director tripod, depending on our needs. Starting from tensors of rank 1:
(l),n
  1
eˆ(1)
(1)
= eˆz , eˆ	= ∓√ (eˆx ± ieˆy ),
(2.1)
0
±1
2
23

Chapter 3. Generalized dispersion model for bent-core systems
24
one can recursively construct tensors of arbitrary rank with the help of Clebsch-Gordan
coefficients:
(

l − 1	1
l
m
\

m1,m2
eˆ(l,δ),n
(l−1),n−1
(1),1
=
eˆm
⊗ eˆm	.
(2.2)
m
1
2
m1
m2
Here δ is the “seniority index”, used to distinguish between linearly independent same-l
tensors within the same Cartesian rank n, which appear for n ≥ 3. From now on we decide to drop the seniority index, except where necessary. Under a rotation R, the irreducible spherical tensor transforms through the Wigner rotation matrix:
\
(l),n (l)
(l),n
Reˆ	=	eˆ	Dm m,
(2.3)
m
m
I	I
mI
(
(l),n\∗
(
(l),n\
(l)
DmIm = eˆm	· ReˆmI	,
(2.4)
where the scalar product “·” is understood as a full contraction over all Cartesian indices.
As one notices from the above expression, a rotation always leaves the tensor in the same l-subspace of angular momentum, thus mixing only tensors with different m. From the many remaining useful properties of irreducible spherical tensors, for the sake of brevity we only name orthonormality between tensors in the same-l subspace. For a comprehensive guide on the properties and construction of spherical tensors and Wigner matrices, cf. e.g. [86].
In the context of liquid crystal research the main advantage from irreducible tensors flows
from symmetry-adaptation. Considering different subgroups of SO(3) (or, in general, O(3)), one can construct irreducible tensors which bear the symmetry of the individual subgroups. The obtained set of tensors gives us complete control over the symmetry in designing the interaction potential and also serves as a neat, symmetry-adapted basis for the alignment tensor. The process of symmetrization is straightforward. If the group in question is G, the G-symmetrized tensor is obtained using the prescription:
1
\
T(l),n
l
(l),n
= cm
O(g)eˆm .
(2.5)
m
|G| g∈G
Here |G| stands for the number of transformations in G and O(g) is the linear operator
associated with transformation g. The coefficients cl are chosen to secure orthonormality
m
of tensors with the same m. In the case of continuous groups, the sum needs to be replaced with SO(3)-invariant integration and |G| is the unit integration volume of the
group.

Chapter 3. Generalized dispersion model for bent-core systems
25
Having at hand the tensors (2.5), we easily produce the complementary symmetrized
Wigner matrices, which we denote ∆(l) , following the notation of Mulder [87]:
mmI
∆(l)
(l),n
= Tm (Ω ) · T	(Ωˆ 2),
(l),n
ˆ
(2.6)
1	mI
mmI
where Ωˆ 1 = {eˆx, eˆy , eˆz } is often identified with the director basis, and Ωˆ 2 is some other
frame of reference, commonly identified with the molecular basis.
Symmetrized tensors form a complete basis for the l-subspace for a given symmetry
group G (a set involving all G-symmetrized tensors for angular momentum l), therefore we have an expansion of the (G-symmetrized) identity operator:
I(l,δ) = \ T(l,δ)
(Ω) ⊗ T	(Ωˆ ).
ˆ
(l,δ)
(2.7)
m
m
G
m,δ
2.1.1
Symmetrized irreducible tensors for selected symmetry groups
For the use in this chapter and for the remainder of this thesis we consider the leading
symmetrized tensors for l = 2 the D2h-symmetrized second rank tensors and for l = 3
the Td-symmetrized third rank tensor.
The non-vanishing l = 2 symmetrized tensors for the biaxial symmetry group D2h, with
symmetry axes coinciding with {eˆx, eˆy , eˆz }, are:
I
3
1
T(2),2
=	(eˆz ⊗ eˆz −	I),
2	3
(2.8)
0
  1
T(2),2
= √2 (eˆx ⊗ eˆx − eˆy ⊗ eˆy )
(2.9)
2
√
(0),2
and the trivial isometric tensor eˆ	= 1/ 3I, where I = eˆ ⊗ eˆ + eˆ ⊗ eˆ + eˆ ⊗ eˆ is the
x
x	y	y	z	z
0
Ωˆ	ˆ
Cartesian identity operator. One recognizes that, when	= {l, mˆ , nˆ}, (2.8) and (2.9)
appear, up to a normalization constant, as components of the alignment tensor (1.18).
∆(2)
Furthermore, the l = 2 D2h-symmetrized Wigner matrix elements
are, up to a
m,mI
(2)
normalization constant, the functions identified by Straley [67], in particular S ∝ ∆0,0)
and T ∝ ∆0,2).
For the tetrahedratic group Td there are no non-vanishing symmetrized tensors of l < 3, apart from trivial isotropic tensors. Distinction by seniority of rank 3 tensors is only needed for tensors of angular momentum l = 2, therefore it can be dropped altogether.
(3),3
(2)
For n = 3, l = 3 there are 7 independent tensors eˆ	, m = −3 . . . 3, and depending on
m
the choice of the symmetry axes, a symmetrized tensor will be a linear combination of
l = 3 tensors with different m. With the choice (that we consider later) that the twofold

Chapter 3. Generalized dispersion model for bent-core systems
26
axes of symmetry coincide with {eˆx, eˆy , eˆz }, the only non-vanishing Td-symmetrized ir-
reducible tensor is [1]:
  1
√6
\
T(3),3
=
eˆi ⊗ eˆj ⊗ eˆk ,
(2.10)
2
(eˆi,eˆj ,eˆk )∈π(eˆx,eˆy ,eˆz )
where the sum runs over all permutations of {eˆx, eˆy , eˆz }.
2.2
Definition of the model
The most general model studied here is a lattice dispersion model, defined by the Hamil-
tonian:
N
\

(i,j)
N
1
2
I
l
VQ(Ωˆ i, Ωˆ j ) + VT (Ωˆ i, Ωˆ j ) + Vc(Ωˆ i, Ωˆ j ) + V T (Ωˆ i, Ωˆ j ) + \ ∆V (Ωˆ i). (2.11)
H =
c
i
The sum runs over nearest neighbors, i.e. for each particle i the sum runs over z = 6
neighboring particles j, while the N particles occupy sites of a simple cubic lattice with periodic boundary conditions (although two other options are considered in Chapter 5). The arguments Ωˆ i and Ωˆ j denote orientations of the particles at lattice sites i and j, which can be expressed equivalently by specifying three orthonormal vectors – the molecular
frame of reference (also: “molecular tripod”, “molecular basis”):	= {aˆi, ˆbi, cˆi} and
Ωˆ i
Ωˆ j
= {aˆj , ˆbj , cˆj }. Note that the molecular frame of reference can be either righthanded
or lefthanded, which will become important when we take a closer look at VT . The
interaction terms are explained as follows:
The quadrupolar term:
VQ(Ωˆ i, Ωˆ j ) = −EQ(Ωˆ i) · Q(Ωˆ j )
(2.12)
couples molecular quadrupolar moments at sites i and j. The scalar product ’·’
is understood as a full contraction over Cartesian indices. The quadrupolar mo- ment Q(Ωˆ i) is a second-rank traceless tensor, which has uniaxial and biaxial parts, defined in terms of irreducible spherical tensors symmetrized with respect to the uniaxial (D∞h) and biaxial (D2h) symmetry groups (2.8-2.9), expressed in the molecular basis:
√
(2)
(2)
ˆ
ˆ
ˆ
Q(Ω ) = T	(Ω ) +	2λT	(Ω ), n = i, j.
(2.13)
n
n
n
0
2

Chapter 3. Generalized dispersion model for bent-core systems
27
The quadrupolar term VQ is responsible for uniaxial and biaxial nematic ordering.
Its history, motivations and previous results are discussed in Chapter 3.
The octupolar term:
•
ˆ	ˆ
(3)
ˆ
(3)
ˆ
V (Ω , Ω ) = −τ ET	(Ω ) · T	(Ω )
(2.14)
T	i	j
i
j
2
2
couples molecular octupolar moments at sites i and j. T(3)(Ωˆ i) is a third-rank
2
irreducible spherical tensor, symmetrized with respect to the tetrahedratic group Td, of the form given in (2.10), expressed in the molecular basis. Together with VQ, this term is shown to be responsible for emergence of phases of tetrahedratic symmetry and spontaneous breaking of chiral symmetry, recently observed experi- mentally. Chirality enters the model through parity (handedness) of the molecular
basis:
pi = aˆi · (ˆbi × cˆi) = ±1,
(2.15)
because a parity switch is a symmetry of Q(Ωˆ i), but not of T(3)(Ωˆ ). In this
2
way, conformations of different chirality are accounted for as microscopic states
parametrized by the parity degree of freedom. Further explanation
Chapter 4.
is
given in
The intermolecular vector coupling terms:
•
Vc(Ωˆ i, Ωˆ j ) = κE [ˆbαi · (ˆbβi × ˆbγi)Qαν (Ωˆ i)Qβν (Ωˆ j )
— ˆbαj · (ˆbβj × ˆbγj )Qαν (Ωˆ j )Qβν (Ωˆ i)l (rˆij )γ,
(2.16)
(3)
2
(3)
ˆ	ˆ
ˆ
ˆ
ˆ
(Ω )T	βνµ(Ωˆ j )
ˆ
V T
(Ω , Ω ) = κ E [ b
(b
× b )T
i	j
T	αi	βi
γi
i
c
2
ανµ
(2.17)
(Ωˆ j )T (3)	(Ωˆ i)l (rˆij )γ,
(3)
2
ˆ
ˆ
ˆ
— b	· (b
× b )T
αj	βj
γj
2
ανµ
βνµ
where α, β, γ, ν = {x, y, z}, Qρδ (Ωˆ ) = (Q(Ωˆ )\
(Ωˆ ) = (T(3)(Ωˆ )\
, T (3)
, ˆbxi =
2
2
αρδ
ρδ
αρδ
aˆi, ˆbyi = ˆbi, ˆbzi = cˆi and Einstein summation convention is implied, couple the
molecular quadrupolar (Vc) and octupolar (V T ) moments to unit vectors rˆij con-
c
necting sites i and j. These terms should be considered because the antisymmetric tensor ˆbαn · (ˆbβn × ˆbγn), n = i, j can be constructed out of the other tensors:
√
\

(x,y,z)∈π{α,β,γ}
ˆbαn · (ˆbβn × ˆbγn) = 2 2
T (2) T (2) T (3)
,
(2.18)
0,xµ 2,yν 2,µνz
(T )
where the summation runs over cyclic permutations of {α, β, γ}. Terms Vc	will
always be generated in the presence of chirality and will lead to an inhomogeneous

Chapter 3. Generalized dispersion model for bent-core systems
28
ground state of the model. (It should be noted that we imply the
resulting in-
homogenities to be of large characteristic lengths when compared to the lattice
spacing.) Further explanation is given in Chapter 5.
The field-coupling term:
•
∆V (Ωˆ i) = −E∆Ehαhβ Q(Ωˆ i)αβ
(2.19)
couples the molecular quadrupolar moment Q(Ωˆ i) to an external, general vector field _h. α, β = {x, y, z} and Einstein’s summation convention is implied in the above definition. E∆E is the anisotropy of the molecular (dielectric or diamagnetic)
field polarizability, where ∆E = ±1, thus the anisotropy is taken equal to the coupling constant in the quadrupolar term VQ above or as a renormalizing factor to the squared field magnitude h2. The origin of this term is further explained in
Chapter 3.
The model (2.11), is designed to reproduce the most remarkable recent findings made in
bent-core systems, ferrocene mesogens and flexible dimers, i.e. biaxial phases [27, 29, 30, 32, 88], spontaneous breaking of chiral symmetry, formation of modulated chiral struc- tures [38–40, 43] including the twist-bend nematic phase [45–50], and tetrahedratic order [51, 52, 54, 55]. In this most general form there are seven independent parameters: the energy scaling parameter E, the biaxiality parameter λ, the tetrahedratic coupling con- stant τ , the intermolecular vector coupling constants κ and κT , the sign of the anisotropy of the molecular field polarizability ∆E and the magnitude of the external field h = |h|. E can be eliminated from the list of free parameters by studying the model with respect to the dimensionless temperature t = kBT/E (which is equivalent to putting E = 1). Fur- thermore, only one of κ and κT needs to be considered, as they generate identical ground states, therefore we choose to disregard κτ . Nevertheless, studying the full spectrum of the remaining five parameters is a large task in itself, but, more importantly, we might have trouble interpreting the results without first studying limit cases. Therefore, this thesis presents a study on several special cases of the general model (2.11). Namely:
_
In Chapter 3 the case of E > 0, λ > 0, h > 0, τ = κ = 0, i.e. the l = 2 model of
biaxial nematics with external field coupling is studied in detail with Monte Carlo simulations and mean-field methods. This limit case, as we will show, produces effects such as field-induced biaxiality in the uniaxial nematic phase, as well as critical and tricritical points of the isotropic-uniaxial nematic transition as the field
1
is increased. For a highly symmetric value of λ =	an external field produces
√6
an unusual effect of reducing the transition temperature and decreasing the level
of biaxiality in a highly-symmetric biaxial phase.

Chapter 3. Generalized dispersion model for bent-core systems
29
In Chapter 4 the case of E > 0, λ > 0, τ > 0, h = κ = 0, i.e. the model proposed in
[1] is studied for selected values of λ and τ with Monte Carlo simulations. This case extends on the studies in [1] by giving full characteristics of homogeneously chiral
28
•
and tetrahedratic structures. In addition, a highly-symmetric value of τ =	is
15
1
studied, for which at λ =	there exists a direct transition from the isotropic to
√6
the chiral phase.
In Chapter 5 selected Monte Carlo simulation results for the case of E > 0, λ >
0, τ > 0, κ > 0, h = 0 are presented. This variant extends on the previous one by accounting for intermolecular vector coupling, which leads to spatially inhomo- geneous phases. We present only preliminary result for this case for 2D and 3D systems. In both cases two distinct structures are identified in the chiral phase, described in more detail in sections 5.3 and 5.4.
•

Chapter 3
Dispersion model of biaxial
nematics in an external field
3.1
Introduction
The possibility of stabilizing a thermotropic biaxial nematic phase in bent-core mesogens
[27, 29] has invigorated the interest in this elusive phase, particularly in the possibility of magnetic or electric field-induced biaxiality [34]. In fact, there are several accounts of field-induced biaxiality in bent-core systems [89–92], apart from numerous results where magnetic or electric field effects produce biaxiality in other systems [93–95]. Although several theoretical descriptions exist [70, 96–98], along with various simulational studies [99–102], a thorough analysis of field-induced effects by a microscopic model appears to be missing. We will now consider a lattice dispersion model of a biaxial nematic liquid crystal interacting with an external vector field, which will be studied with mean-field and Monte Carlo methods. This chapter completes the preliminary results first published in [103].
3.2
Dispersion models of biaxial nematics
The idea of a biaxial nematic phase first occurred to Freiser in 1970 [21]. He asserted
that for correct description of biaxial systems the l = 2 subspace needs to be considered in the multipole expansion of pair dispersion interaction energy and predicted that a sequence of a first-order transition to the uniaxial nematic and second-order transition to the biaxial nematic should occur with lowering temperature.
31

Chapter 4. Dispersion model of biaxial nematics in an external field
32
In 1974 Straley [67] considered a generalization of the Maier-Saupe pair potential (1.9)
constructed on D2h-symmetry-adapted functions for l = 2. Assuming a system of brick- like objects of length L, breadth B and width W , using mean-field methods he produced the phase diagram for objects of varying breadth. It appears so that there exists a special
value of B = √LW , corresponding to maximum biaxiality, where the transition from the
isotropic phase is directly into the biaxial phase. Furthermore, Straley noticed that the models for rodlike (B < √LW ) and platelike objects (B > √LW ) can be mapped onto each other through a duality transformation. At B = √LW the transformation carries the model into itself, therefore B = √LW has been named the “self-dual” point.
Similarly to Freiser, Luckhurst and Zannoni considered a l = 2 expansion of the point dispersion potential in Wigner rotation matrices DmmI and developed a molecular field model [63]. Monte Carlo simulation for a l = 2 model has been first performed by Luckhurst and Romano [64]. Their version introduced the parameter λ, which controls the biaxiality of molecules, closely related to Straley’s B. Namely, 0 ≥ λ ≤ 2 , while the boundary cases correspond to Maier-Saupe-like uniaxial models for long rods (λ = 0)
(2)
I 3
and platelets (λ = I 3 ). The case of maximum biaxiality is represented by λ =	. The
1
√6
2
phase diagram for varying λ has been obtained using mean-field theory and supported
by Monte Carlo simulations by Biscarini et al. in 1995 [104]. Thorough Monte Carlo investigation of the self-dual point has been performed by Chiccoli [105].
The l = 2 model family has been studied and reformulated extensively. Mulder explored
∆(2)
the expansion in terms of symmetry-adapted functions
with bifurcation theory
mmI
[87]. A version of the model has been studied by Sonnet et al. [106] and Bisi et al. [107]
for which an universal mean-field phase diagram has been obtained. Density functional and bifurcation theory has been analyzed by Longa et al. [108]. In parallel, comprehen- sive Landau-de Gennes theory has been developed by Palffy-Muhoray and Dunmur [96], Allender [109], Gramsbergen et al. [70] and more recently by Allender and Longa [72]. Longa and Pająk further analyzed the link between phenomenological theory and the l = 2 Luckhurst-Romano model [71].
3.2.1
Dispersion model of interacting quadrupoles
The base for our model is the Luckhurst-Romano model expressed in the parametrization
of irreducible spherical tensors. In this model it is assumed that the dispersion interaction is due to coupling of induced quadrupolar moments. In the general model (2.11), this model corresponds to the case where all parameters aside from λ and E are zero. The

Chapter 4. Dispersion model of biaxial nematics in an external field
33
pair potential and Hamiltonian read:
VQ(Ωˆ i, Ωˆ j ) = − EQ(Ωˆ i) · Q(Ωˆ j ),
N
(3.1)
1
H = \ VQ(Ωˆ i, Ωˆ j ),
2
(i,j)
where E > 0 and Ωˆ i = {aˆi, ˆbi, cˆi} and Ωˆ j = {aˆj , ˆbj , cˆj } specify orientations of the molec- ular frames of reference with respect to the laboratory frame of reference {xˆ, yˆ, zˆ} for molecules i and j respectively (see Fig. 3.1a). The sum runs over nearest neighbors, i.e. for every i we take z = 6 neighboring particles on a simple cubic lattice with periodic boundary conditions. The scalar product “·” is understood as a full contraction over all
The quadrupolar molecular moment Q(Ωˆ i) is a second-rank tensor,
Cartesian indices.
defined as:
√
ˆ
(2)
ˆ
(2)
ˆ
Q(Ω ) = T	(Ω ) + λ 2T	(Ω ).
(3.2)
i
i
i
0
2
I 3
λ ∈ [0,	2 ] is a parameter which controls molecular biaxiality by combining T0 (Ωˆ i)
(2)
and T(2)(Ωˆ i) – the second-rank D
and D -symmetrized irreducible spherical tensors
∞h
2h
2
for l = 2, previously defined in (2.8-2.9), which here are constructed in the molecular
basis Ωˆ i:
I
3
1
T(2)
(Ωˆ i) =	(cˆi ⊗ cˆi −	I),
2	3
  1
0
(3.3)
T(2)
(Ωˆ i) =	√ (aˆi ⊗ aˆi − ˆbi ⊗ ˆbi).
2
2
As the interaction (3.1) is regarded as the leading part of the intermolecular dispersion
interaction, Q(Ωˆ ) can be interpreted as being proportional to the anisotropic part of the molecular (dielectric or diamagnetic) polarizability tensor α. In this case, the parameters
E and λ are related to the diagonal elements of the diagonalized tensor α {αx, αy, αz }:
I
αx−αy
3
2
E = E (2α − α − α ) , λ =
.
0	z
x
y
2 2αz −αx−αy
If one expresses (3.1) using the symmetry-adapted Wigner functions (2.6) for l = 2, by
substituting Ωˆ 1 = Ωˆ i and Ωˆ 2 = Ωˆ j , the pair potential reads:
I
√
l
(2)
(2)
(2)
(2)
ˆ	ˆ
ˆ
ˆ
ˆ
ˆ
2
V (Ω , Ω ) = −E ∆	(Ω ) +	2λ[∆	(Ω ) + ∆	(Ω )] + 2λ ∆	(Ω ) ,
(3.4)
Q	i	j
ij
ij
ij
ij
00
20
02
22
which is the parametrization of the model as presented in [64] and [104]. Clearly, the
minimum of (3.1) is achieved when all of the respective molecular axes of Q(Ωˆ i) and
Q(Ωˆ j ) coincide, i.e. when:
aˆi aˆj , ˆbi ˆbj , cˆi cˆj .
Thus, the ground state of (3.1) is the biaxial nematic phase NB (Fig. 3.1b).
(3.5)

Chapter 4. Dispersion model of biaxial nematics in an external field
34
a
b
Figure 3.1: Visualization of molecular quadrupolar moments Q(Ωˆ i) and Q(Ωˆ j ) (3.2) at neighboring lattice sites i and j, located at _ri and _rj , for:
a) exemplary orientations of the molecular tripods Ωˆ i = {aˆi, ˆbi, cˆi} and Ωˆ j = {aˆj , ˆbj , cˆj }
with respect to the laboratory frame of reference {xˆ, yˆ, zˆ};
b) a ground state of the potential (3.1), in which aˆi aˆj , ˆbi ˆbj , cˆi cˆj .
The molecular axes are scaled by the magnitudes of the corresponding eigenvalues of the molecular quadrupolar tensors (a red arrow denotes a negative eigenvalue). The pictured quadrupolar tensors are for λ = 0.3.
3.2.1.1	Properties of Q(Ωˆ )
Consider a molecular tensor Q(Ωˆ ) constructed in the molecular basis	= {aˆ, ˆb, cˆ} for
Ωˆ
an arbitrary particle. Since this tensor is traceless, we cannot directly equate its eigen-
values with spatial dimensions of a tangible object. To establish an intuitive framework, from now on we adopt a convention that the sign of the largest-modulus non-degenerate eigenvalue of Q(Ωˆ ) specifies the molecular long axis (+) or the largest face (−). The axis corresponding to this eigenvalue is considered the primary molecular axis, while the second largest-modulus eigenvalue (if non-degenerate) identifies the secondary molecular axis. In the diagonal form, Q(Ωˆ ) reads:


1
−√6 + λ
0
0
0
0

0  R
ˆ
T
1
—	− λ
Q(Ω) = R
,
(3.6)
√6
0
{aˆ,ˆb,cˆ} 

	{aˆ,ˆb,cˆ}

I 2
3
where R{aˆ,ˆb,cˆ} is a rotation matrix, carrying the laboratory frame to the molecular frame
of reference. From the above form we can now see that in the limit cases of the pa-
rameter λ ∈ [0,	2 ] a uniaxial tensor is recovered. Namely, for λ = 0 the eigenvalues
I 3

Chapter 4. Dispersion model of biaxial nematics in an external field
35
a
b
c
Figure 3.2: Visualizations of the molecular tensor Q(Ωˆ ) and its eigenvalues in the di-
1
1
1
agonal basis for a) λ <	, b) λ >	and c) λ =	. The vectors are scaled by
√6
√6
√6
magnitudes of corresponding eigenvalues. A red arrow means that the corresponding
eigenvalue is negative. Surface described by r = exp (Q · uˆ ⊗ uˆ) where uˆ is a unit vector in polar coordinates.
I
, so that Q(Ωˆ ) is degenerate in the {aˆ, ˆb}
1
1	2
are {−	, −	,	}
-plane and cylindrically
√6
√6
3
symmetric along cˆ. The largest-modulus non-degenerate eigenvalue corresponds to cˆ and
is positive. Therefore, this case corresponds to the prolate molecule with primary axis cˆ. (See Fig. 3.2a.)
I
I
I	I
3
2
2 ,	2
Conversely, if λ =	, the eigenvalues are {	, −2
}, axes {aˆ, cˆ
} are degenerate
2
3
3	3
and the largest-modulus non-degenerate eigenvalue is negative and corresponds to ˆb.
Thus, the corresponding molecular shape is a flat disk with primary axis ˆb. (See Fig.
3.2b.)
I	I
1
2	2
In the self-dual point λ =	, the eigenvalues are {0, −	,	} and, while non-
√6
3	3
degenerate, the axes ˆb and cˆ are equivalent. The corresponding object has both a pro- found long axis, identified by cˆ, and a large face, identified by ˆb. This case corresponds
to biaxial bricks of dimensions (L, √LW, W ), as identified by Straley. (See Fig. 3.2c.)

Chapter 4. Dispersion model of biaxial nematics in an external field
36
3.2.1.2
Duality transformation
The duality transformation for model (3.1) is performed by simultaneously rescaling both
λ and the dimensionless temperature t ≡ kBT/E, while cyclically permuting the axes such that {aˆ, ˆb, cˆ} → {cˆ, aˆ, ˆb} [108]:
I
3
2 − λ
λ →

t →
1 + √6λ
(3.7)
4t
(1 + √6λ)2 .
Such transformation leaves the Boltzmann factor e−H/t invariant. (3.7) is identity when
1
λ =	.
√6
3.2.1.3
Phases and phase transitions
The isotropic-uniaxial nematic phase transition is of first order, occurring through spon-
taneous breaking of the global rotational symmetry of the Hamiltonian (3.1), as in the Maier-Saupe and Lebwohl-Lasher models. In the uniaxial nematic phase the long-range ordering is of the molecular axis corresponding to the largest-modulus eigenvalue of
Q(Ωˆ ). Therefore, a nematic prolate
1
NU +
phase is observed for λ <	and a nematic
√6
  1
oblate
NU −
is observed for λ >
√6 ,
with the primary uniaxial director nˆ due to the
long-range ordering of the cˆ and ˆb axes respectively. For these cases, as the temperature
is lowered in the nematic phase, a second-order phase transition to the biaxial nematic
1
NB phase occurs, through spontaneous breaking of uniaxial symmetry. At λ =	nei-
√6
ther of cˆ and ˆb is privileged and ordering of both is simultaneous, hence there is a direct
transition from the isotropic (I) to the biaxial nematic phase (NB ), known to be second order [104, 105]. The phase diagram for the model (3.1) is presented in Fig. 3.3.

Chapter 4. Dispersion model of biaxial nematics in an external field
37
Figure 3.3: Phase diagram for model (3.1) in the plane (λ, T ∗ =
kBT/E), obtained
by Biscarini et al. [104]. Points denote Monte Carlo simulation results, while lines
1
correspond to mean-field predictions. At the self-dual point λ =	≈ 0.408248 there
√6
exists a direct isotropic-biaxial nematic second order transition. Here the symbols I,
N+, N− and B stand for the isotropic, nematic uniaxial prolate, nematic uniaxial oblate
and nematic biaxial phases, throughout the present text denoted as I, NU +,
NU −
and
NB respectively. Reprinted FIG. 2 with permission from F. Biscarini, C. Chiccoli, P.
Pasini, F. Semeria, and C. Zannoni. Physical Review Letters, 75 (9):1803–1806, 1995. Copyright 1995 by the American Physical Society.)

Chapter 4. Dispersion model of biaxial nematics in an external field
38
3.3
Dispersion model with external field
In nematic liquid crystals application of an external electric or magnetic field affects the
orientation of the sample [2, cc. 3.2-3.3]. Most nematogenic molecules are diamagnetic, as they in general contain one or more benzene rings (e.g. MBBA, see Fig. 3.4), which respond to the application of an external magnetic field by an induced repellent eddy current, if the field is at an angle to the benzene ring plane. Therefore, in the case of magnetic fields, the effect works generally to adjust the director _n to align in parallel to the external magnetic field H_ .
O
N
Figure 3.4: N-(4-Methoxybenzylidene)-4-butylaniline (MBBA) (Qc Wikimedia Commons,
Creative Commons CC0 1.0 Universal Public Domain Dedication)
The magnetization induced in a nematic sample by an external magnetic field H_ reads:
M_
H_
− χ )(H_ · _n)_n.
= χ	+ (χ
(3.8)
⊥
l	⊥
χl and χ⊥ are the anisotropic components of the bulk diamagnetic polarizability tensor,
corresponding to the long molecular axis and the axis perpendicular to benzene ring plane. The difference ∆χ = χl − χ⊥ is the diamagnetic anisotropy of the sample. The
corresponding contribution to energy is given by:
r
H
1
1
M_
· dH_ = − 2 χ⊥H − 2 ∆χ(_n · H_ ) .
2
2
∆EM = −
(3.9)
0
The first term is independent of _n, so it can be discarded. The second term promotes
_n H_ if ∆χ > 0 and _n ⊥ H_ if ∆χ < 0. For uniaxial nematics the alignment tensor is
1
Q = S(_n ⊗ _n − I), so the second term can be rewritten:
3
r
2
1
1
1
− 2 ∆χ(_n · H_ ) = − 2 ∆χ HiHj Qij + 3 H	,
2
(3.10)
where i, j = {x, y, z}. Again, the term proportional to H2 can be dropped, and we have:
1
∆El = − 2 ∆χHiHj Qij.
(3.11)
M
A similar term to (3.11) appears when the electric field is considered instead.

Chapter 4. Dispersion model of biaxial nematics in an external field
39
3.3.1
Model
A similar discussion to (3.8-3.11) can be conducted at the microscopic level. The contri-
bution to the potential energy of particle i then reads [70]:
∆V (Ωˆ i) = −E∆Ehαhβ Q(Ωˆ i)αβ.
(3.12)
We distinguish the general vector field _h because of the universal character of (3.12),
which can also express interaction with an electric field (to an extent where piezoelectric effects can be neglected [110]). The analogue of bulk diamagnetic anisotropy is the anisotropy of the molecular (dielectric or diamagnetic) field polarizability, E∆E. In our discussion we distinguish only the sign of the anisotropy of the field polarizability and let ∆E = ±1, either assuming that the anisotropy is equal to the quadrupolar coupling constant E, or that it renormalizes h2. Note that we use the full biaxial molecular tensor Q(Ωˆ ), as defined in (3.2), and assume a proportionality for the molecular polarizability tensor for particle i:
ˆ
χi
∝ E∆EQ(Ω )	,
(3.13)
i αβ
αβ
which is a model assumption. Together with (3.1), the dispersion model for biaxial
nematics in the presence of an external vector field is given by the Hamiltonian:


N
N

1 \
\
H = −E  2	Q(Ωˆ i) · Q(Ωˆ j ) + ∆E	hαhβ Q(Ωˆ i)αβ  .
(3.14)
(ij)
i
We take the first sum over the nearest neighbors, i.e. for every i we take only z = 6
neighboring particles on a simple cubic lattice with periodic boundary conditions. This model corresponds to the general model (2.11) for the case when the parameters λ, E and h are non-zero. In our discussion we will assume that the model (3.14) is studied with respect to a dimensionless temperature t ≡ kBT/E (which is equivalent to putting E = 1).
3.3.2
Field-induced effects
While the model (3.1) has global rotational symmetry, in the model with non-zero exter-
nal field (3.14) the rotational symmetry is broken by definition. Therefore, the Hamil- tonian (3.14) has global symmetry with respect to rotation around the vector _h, which determines the preferred alignment of one of the molecular axes and, consequently, one of the directors. Considering a sample particle for which the orientation is given by
Ωˆ
= {aˆ, ˆb, cˆ}, there are two main microscopic effects, consistent with the minima of
(3.12), when h /= 0, namely:

Chapter 4. Dispersion model of biaxial nematics in an external field
40
for ∆E = +1 the molecular cˆ axis (which corresponds to the largest, with respect
to the modulus, positive eigenvalue of Q(Ωˆ ), regardless of λ) aligns parallel to _h (Figs. 3.5a and c);
for ∆E = −1 the molecular ˆb axis (which corresponds to the largest, with respect to the modulus, negative eigenvalue of Q(Ωˆ ), regardless of λ) aligns parallel to _h (Figs. 3.5b and d).
What precisely happens to the orientation of the director basis depends on λ and the
considered zero-field phase, to which a non-zero field is introduced. We identify two classes of macroscopic effects, distinguished by how the field affects the director of the zero-field uniaxial nematic phase. Namely, considering the above discussion of the ori- entation of molecular axes, the field can make the primary uniaxial director nˆ either parallel or perpendicular to _h. In the first case, the field reinforces uniaxiality, while in the second case biaxiality is induced, because the field forces rotation of the uniaxial director nˆ to align perpendicularly to _h and orients the secondary molecular axis (and therefore the secondary director mˆ ) in parallel to _h.
1
1
The uniaxiality-promoting effect occurs for λ <
(Figs. 3.5a and b).
∧ ∆E = +1 or λ >
∧ ∆E = −1
√6
√6
1
1
The biaxiality-promoting effect occurs for λ <
(Figs. 3.5c and d).
∧ ∆E = −1 or λ >
∧ ∆E = +1
√6
√6
3.3.2.1
Uniaxiality-promoting effects
1
1
Cases of λ <
∧ ∆E = +1 (Fig. 3.5a) and λ >	∧ ∆E = −1. (Fig. 3.5b).
√6
√6
A non-zero field aligns the director nˆ parallel to the field in all phases for this particular
case. Firstly, in the isotropic phase the field induces uniaxial ordering. The increase in uniaxiality (e.g. in the uniaxial order parameter S, as defined in (1.2)) is proportional to h2 and the resulting phase is called paranematic. Depending on λ this uniaxial phase
1
1
can be either prolate (NP +) for λ <	, or oblate (NP ) for λ >	.
√6
√6
−
When considering the zero-field uniaxial nematic phase, the uniaxial ordering is increased
by the application of the field. The NP − NU phase transition is of first order. It is known that the transition temperature rises with increased field and it is predicted by phenomenological theories that the transition should terminate at a critical point [70, 96].
In the biaxial nematic phase the field does not reduce symmetry, although Landau-de
Gennes theory predicts that the NU − NB transition temperature may either increase or decrease [103].

Chapter 4. Dispersion model of biaxial nematics in an external field
41
a
b
c
d
Figure 3.5: Visualizations of the minima of (3.12) for cases:
1
a) λ <	∧ ∆E = +1,
√6
1
b) λ >	∧ ∆E = −1,
√6
1
c) λ <	∧ ∆E = −1,
√6
1
d) λ >	∧ ∆E = +1.
√6
The arrows represent eigenvectors of Q(Ωˆ ) and are scaled by the magnitudes of respective eigenvalues. A red arrow means that the corresponding eigenvalue is negative. The dashed arc illustrates the degeneracy of the minimum in the plane perpendicular to _h. Surface described by r = exp (Q · uˆ ⊗ uˆ), where uˆ is a unit vector in polar coordinates.
3.3.2.2
Biaxiality-promoting effects
1
1
Cases of λ <
∧ ∆E = −1 (Fig. 3.5c) and λ >	∧ ∆E = +1. (Fig. 3.5d).
√6
√6
In the isotropic phase the field orients the director nˆ parallel to the field, as in the
1
previous case. Depending on λ, the paranematic prolate phase (NP +) occurs for λ >
√6
  1
and the paranematic oblate phase (NP −) is found for λ <
√6 .
In the uniaxial nematic phase the field forces the director nˆ to align in perpendicular to _h
and biaxiality is induced, with the secondary director mˆ parallel to _h. Upon the NP −NB transition, the director nˆ is reoriented from being parallel to _h to being perpendicular to hˆ. This transition is initially first-order, but is predicted by phenomenological theories to experience a tricritical point for high enough fields and then to continue as second-order [70, 96], when the field is sufficiently large so that field-ordering becomes dominant.

Chapter 4. Dispersion model of biaxial nematics in an external field
42
The biaxial nematic phase, which exists for no field, blends seamlessly with the biaxial
nematic phase which is induced in place of the uniaxial nematic. The NU −NB transition, being second order, simply vanishes as the field is introduced, leaving a smooth increase in biaxial ordering as temperature is lowered.
1
3.3.2.3
Field effects for λ =
√6
The self-dual point is a special case because of the high symmetry involved. For h = 0 the
molecular axes cˆ and ˆb are equivalent and there is no director along which the uniaxial ordering is predominant, as it can only be field-induced. For h /= 0 cˆ is preferred to align in parallel to _h for ∆E = +1, while ˆb is preferred to align in parallel to _h for ∆E = −1. In the isotropic phase, this induces a paranematic prolate (NP +) phase and a paranematic oblate (NP −) phase in the respective cases. In the self-dual case the biaxial nematic phase for h = 0 is a phase with maximum biaxiality (that is, the alignment tensor has no uniaxial part), in which the induced uniaxial ordering for h /= 0 can actually reduce the level of biaxial ordering, thus lowering the NP − NB transition temperature.
3.3.3
Duality transformation
The discussed field-induced effects hint upon a symmetry of the model (3.14) with respect
to the permutation of molecular axes and a change of λ from the prolate to the oblate case, coupled with a switch in the sign of ∆E. Such self-dual transformation for (3.14) is performed by extending on the transformation (3.7) for model (3.1) by simultaneously rescaling also the magnitude of the field. Namely, the argument of the Boltzmann factor
is invariant when the axes are cyclically permuted such that {aˆ, ˆb, cˆ} → {cˆ, aˆ, ˆb}
e−H/t
and dimensionless temperature t = kBT/E, λ and ∆Eh2 are rescaled:
I 3
2 − λ
λ →
1 + √6λ
4t
(1 + √6λ)2
.
(3.15)
t →
2
−2∆Eh
∆Eh2 →
1 + √6λ

Chapter 4. Dispersion model of biaxial nematics in an external field
43
3.4	Tools and methods
3.4.1	Order parameters
3.4.1.1
Alignment tensor
The description of order in biaxial nematics is primarily achieved by investigating the
properties of the alignment tensor, which, similarly to the molecular quadrupolar mo- ment, is composed of uniaxial and biaxial contributions:
√
(2)
(2)
Q ≡ T0 (Ωˆ l) +	2λT2 (Ωˆ l),
(3.16)
where the overline denotes the ensemble average and Ωˆ l is, as of yet, an unspecified cyclic permutation of the molecular basis {aˆ, ˆb, cˆ}, for which there are three possibilities. The
(2)
ˆ
ˆ
tensors T	(Ω ), m = 0, 2 are constructed by assuming {
l
eˆ , eˆ , eˆ } ≡ Ω in the definitions
l
m
x	y	z
(2.8-2.9). The proper choice of Ωˆ l, for which a consistent Q is obtained, is made such that
the average uniaxial tensor T(2)(Ωˆ l) and the average biaxial tensor T(2)(Ωˆ l) unequivocally
0
2
determine the primary uniaxial director nˆ and the two secondary (biaxial) directors mˆ
and	respectively, consistently with the qualitative predictions made in the previous sections, depending on the field _h and parameters λ and ∆E:
ˆl
1
For λ /=	the appropriate uniaxial tensor is the one constructed upon the primary
•
√6
molecular axis (while the biaxial tensor is built out of the remaining two), thus
Ωˆ l = {aˆ, ˆb, cˆ} for λ <	and Ωˆ l = {cˆ, aˆ, ˆb} for λ >	.
1
1
√6
√6
ˆ
ˆ
1
For λ =	and h = 0 in the biaxial phase the only viable choice is Ω = {b, cˆ, aˆ},
l
•
√6
ˆ
for which the biaxial tensor is constructed using the (equivalent) axes cˆ and b. In
the other two options one of them is being distinguished completely artificially.
(2)
ˆ
ˆ
The average uniaxial tensor T	(Ω = {b, cˆ, aˆ}
) is purely uniaxial and is non-zero
l
0
only because the ordering of cˆ and ˆb necessarily causes ordering of aˆ.
1
For λ =	and h /= 0 the field prefers rotation of one of the molecular axes parallel
•
√6
to _h, i.e. cˆ for ∆E = +1 and ˆb for ∆E = −1. In this case the average of T(2)(Ωˆ l)
0
Ωˆ l
ˆ
with the choice of	= {b, cˆ, aˆ}, as for h = 0, is not consistent with the uniaxial
director and also does not account for the increase in uniaxial ordering along _h. Therefore, Ωˆ l = {aˆ, ˆb, cˆ} for ∆Eh2 > 0 and Ωˆ l = {cˆ, aˆ, ˆb} for ∆Eh2 < 0.

Chapter 4. Dispersion model of biaxial nematics in an external field
44
In conclusion, the alignment tensor which is consistent with the qualitative predictions
is defined as:
  1
  1

√
(2)
(2)
 T0 ({aˆ, ˆb, cˆ}) +	2λT2 ({aˆ, ˆb, cˆ}) for λ <
2
and λ =
∧ ∆Eh > 0

∧ ∆Eh2 < 0 .
√
√
6
6


  1
  1

√
(2)
(2)
T0 ({cˆ, aˆ, ˆb}
) +	2λT2 ({cˆ, aˆ, ˆb}) for λ > √
and λ = √
Q ≡
6
6

1
√

 T(2)
(2)
ˆ
ˆ
({b, cˆ, aˆ}) +	2λT2 ({b, cˆ, aˆ}) for λ = √6 ∧ h = 0

0
(3.17)
By following the definition (3.17), we can calculate the director frame of reference
{l, mˆ , nˆ} as the eigenbasis of Q, identifying the directors by the moduli of its respec- tive eigenvalues:
ˆ
ˆ
{l, mˆ , nˆ} : {|ωˆl| ≤ |ωmˆ | ≤ |ωnˆ |}.
(3.18)
Because in (3.17) the averaged tensors are traceless, also Tr(Q) =
ωnˆ + ωmˆ
+ ωˆl = 0.
The properties of the phase in which Q is measured can be inferred from the eigenvalues:
In the isotropic (I) phase ωnˆ = ωmˆ = ωˆl = 0 (no directors can be identified).
In the uniaxial nematic or paranematic prolate phase (NU + or NP +), ωnˆ > 0, ωmˆ =
ωˆl = −ωnˆ /2 (nˆ is well-defined, while Q is degenerate in the {l, mˆ } plane).
In the uniaxial nematic or paranematic oblate phase (NU − or NP −), ωnˆ < 0, ωmˆ =
ωˆl = −ωnˆ /2 (nˆ is well-defined, while Q is degenerate in the {l, mˆ } plane).
•
•
ˆ
•
ˆ
1
In the biaxial nematic phase for (NB ) for λ /=	,	/= ωmˆ , ωˆ = −(ωnˆ + ωmˆ )
ωnˆ
•
√6
l
1
(all three directors are well-defined). For the isolated case of λ =	∧ h = 0,
√6
ωnˆ = −ωmˆ , ωˆl = 0 (directors nˆ and mˆ are interchangeable).
In addition, we can use the invariant parameter w, as defined in (1.21), which takes
different values in the various phases: w = +1 in prolate phases (NU + or NP +), w = −1 in oblate phases (NU − or NP −) and |w| < 1 in the biaxial nematic phase (NB ). In particular w = 0 in the maximally biaxial phase. In the isotropic phase w is undefined.
•

Chapter 4. Dispersion model of biaxial nematics in an external field
45
3.4.1.2
Definition of order parameters
The natural order parameters are the coefficients for decomposing
symmetrized irreducible tensors in the director basis:
Q in the basis of
I
3
1
T(2)
ˆ
({l, mˆ , nˆ}) =	2 (nˆ ⊗ nˆ − 3 I)
({l, mˆ , nˆ}) =	√2 (l ⊗ l − mˆ ⊗ mˆ ).
0
(3.19)
  1 ˆ
T(2)
ˆ
ˆ
2
The decomposition is constructed using the D2h-symmetrized identity operator (2.7) for
l = 2 (for which case the seniority index is irrelevant), constructed in the director basis:
\

m=0,2
ˆ
ˆ
(2)
(2)
Q =
Q · T	({
l, mˆ , nˆ}) ⊗ T	({
l, mˆ , nˆ}),
(3.20)
m
m
where the coefficients:
(2)
ˆ
q0 = Q · T0 ({l, mˆ , nˆ})
q2 = Q · T2 ({l, mˆ , nˆ})
are the uniaxial (q0) and biaxial (q2) order parameters, normalized such that |q0| ∈ [0, 1]
and |q2| ∈ [0, √2λ]. With these parameters we can express the eigenvalues of Q, i.e.:
(3.21)
(2)
ˆ
I 2
q0	q2
q0	q2
{ωnˆ =	3 q0,	= −√6 − √2 , ωˆl = −√6 + √2 }.
ωmˆ
(3.22)
From the eigenvalues of Q (3.22) and the discussion from the previous section we infer
the following properties of the order parameters:
In the isotropic (I) phase q0 = q2 = 0.

In the uniaxial nematic or paranematic prolate phase (NU + or NP +), q0 > 0, q2 = 0.

- In the uniaxial nematic or paranematic oblate phase (NU − or NP −), q0 < 0, q2 = 0.
- In the biaxial nematic phase (NB ) either q0 > 0, q2 < 0 or q0 < 0, q2 > 0, which is enforced by Tr(Q) = 0.
3.4.1.3
Invariant parameter w
In the cases where the increases in ordering are very small, as in the field-induced NP
phases, the invariant parameter w (1.21), as introduced in section 1.6, provides unequiv- ocal identification of the phase, assuming a value of ±1 for arbitrarily small uniaxial

Chapter 4. Dispersion model of biaxial nematics in an external field
46
ordering. Expressed through order parameters (3.21), the parameter reads:
q3
2
0 − 3q0q2
w =
(q2 + q2)3/2 .
(3.23)
0	2
3.4.2
Mean-field method
By applying the formalism recollected in section (1.7) to the potential of the model (3.14),
we write the mean-field equations, which enable us to calculate the order parameters q0
and q2. The effective potential is obtained as follows:
z=6
Veff (Ωˆ ) = −E \ Tr IPeq (Ωˆ i)Q(Ωˆ i) · Q(Ωˆ )l = −EzQ · Q(Ωˆ ),
(3.24)
Ωˆ i
i
where z is the coordination number (number of nearest neighbors) and	= {aˆ, ˆb, cˆ} is
the orientation of the molecular basis for a sample particle, expressed with respect to the
Ωˆ
laboratory frame of reference. By applying the decomposition of the alignment tensor
(3.20) to (3.24), we obtain:
(2)
(2)
ˆ
ˆ
ˆ
ˆ
V
(Ω) = −Ez[q T	({l, mˆ , nˆ}) + q T	({l, mˆ , nˆ})] · Q(Ω).
(3.25)
eff
0
2
0
2
The above definition can be explicitly expressed in terms of symmetrized Wigner func-
tions, discussed in section 2.1:
∆(2)
(2)
ˆ
ˆ
ˆ
(2)
(Ω) = T	({l, mˆ , nˆ}
) · T	(Ω),
(3.26)
m
mmI
mI
ˆ
ˆ
where we use the definition (2.6), substituting the director basis for Ω ≡ {l, mˆ , nˆ} and
1
the molecular basis for a sample particle for Ωˆ 2 ≡ {aˆ, ˆb, cˆ}. Using (3.26) in (3.25), while observing the form for the tensor Q(Ωˆ ) (3.2), we obtain:
I	(
√
\
(
√
\l
(2)
(2)
(2)
(2)
ˆ
ˆ
ˆ
ˆ
ˆ
V
(Ω) = −Ez q	∆	(Ω) +	2λ∆	(Ω) + q	∆	(Ω) +	2λ∆	(Ω)	.	(3.27)
eff
0
2
00
02
20
22
The complete mean-field Hamiltonian and equilibrium free energy per particle read:
HMF (Ωˆ )
f = F/N
= Vef (Ωˆ ) − E∆Ehαhβ Q(Ωˆ )αβ,
(3.28)
(3.29)
z
2
2
=	(q + q ) − t log Z.
0
2
2

Chapter 4. Dispersion model of biaxial nematics in an external field
47
The mean-field partition function and equilibrium particle distribution function are given
by:
r
dΩˆ e−βHMF (Ωˆ ),
Z
=
(3.30)
ˆ
Peq (Ωˆ )
Z−1e−βHMF (Ω),
=
(3.31)
where β = (kBT )−1. The order parameters can be calculated as mean-field averages of
combinations of symmetrized Wigner functions, as given below:
r
(
√
\
(2)
(2)
ˆ
ˆ
ˆ
ˆ
q0 =
dΩP
(Ω) ∆	(Ω) +	2λ∆	(Ω) ,
eq
00
02
(3.32)
r
(
√
\
(2)
(2)
ˆ
ˆ
ˆ
ˆ
q2 =
dΩP
(Ω) ∆	(Ω) +	2λ∆	(Ω) .
eq
20
22
q0 and q2 are obtained using two methods, described in the paragraphs that follow.
3.4.2.1
Self-consistent approach
In the first procedure the equations (3.30-3.32) are solved iteratively. We parametrize Ωˆ with Euler angles and the integration is carried out using a Monte Carlo method with importance sampling, through the Vegas algorithm from the Cuba Library, version 2.1 [111]. The initial values of parameters q0 and q2 for a given temperature t are supplied randomly with a uniform distribution on [−1, 1], and subsequently we observe which seed yields convergence to the lowest free energy per particle f (3.29). The equations are iterated until the variance of the last 10 iterations drops below 10−10. It typically takes 20 ∼ 30 iterations for convergence when t is far from the transition temperature, while as much as 100 ∼ 200 iterations are needed in the phase transition vicinity. Because the integration is approximate, the behavior of order parameters is correctly recovered only away from transition temperature, while in the vicinity of the phase transition the order parameters are smoothed out, which makes this method impractical for distinguishing between transitions of different order. However, the self-consistent method is very useful in studying the NU − NB transition, for which the order is known. This transition occurs at relatively low temperatures, where the high-temperature expansion method, discussed below, proves difficult to apply. With the self-consistent method we successfully perform calculations for (dimensionless) temperatures as low as 0.1. It should be noted, however,
that anything that is obtained in such low temperatures is only a property of the model,
|t−tINU |
since real nematic phases are stable for higher temperatures, for which
� 0.2,
tINU
where tINU is the temperature of the isotropic to nematic uniaxial phase transition.

Chapter 4. Dispersion model of biaxial nematics in an external field
48
3.4.2.2
High-temperature expansion
t−1
We expand the mean-field partition function (3.30) around βE =	= 0 (t
being the
dimensionless temperature) in the expression for the mean-field free energy per particle
(3.29):

\
\i
n
r
z
i 1
 (
i!
fn = 2 (q0 + q2 ) − t log	dΩˆ
ˆ
2	2
t−
HMF
(Ω)	.
(3.33)
−
i=0
The procedure is to choose a suitable expansion order n and integrate term-by-term,
leaving q0 and q2 as free parameters. The terms are integrable polynomials in trigono- metric functions of Euler angles. q0 and q2 are found for a given t by minimization of the resulting approximate free energy per particle fn:
∂

f =
0
n
 ∂q0


 ∂
fn =
0

 ∂q2
∂2
(3.34)
fn >
0

	2
∂q
	0
∂2
2


f >
0.

n

∂q
2
We use n = 6 through n = 14 as needed. Because of the factor t−i, the series in (3.33) converges very slowly in low temperatures, where higher terms become important and even for orders as high as n = 14 the approximation breaks down at t ≈ 0.8, which (save
1
for the vicinity of λ =	) is usually much higher than the NU − NB transition. On the
√6
other hand, in t > 1, as few as n = 6 terms provide a very good approximation, therefore the expansion (3.33) proves very useful in studying the I − NU transition. Because the leading terms are exact and not approximated, as in the self-consistent method from the previous section, the expansion method correctly recovers order parameter discontinuities
at the first-order phase transition.
3.4.3
Monte Carlo simulations
We assume a simple cubic lattice of N = 16 × 16 × 16 particles with periodic boundary
conditions. Each molecule interacts only with the z = 6 nearest neighbors. For each separate temperature the simulation runs independently, starting from a completely bi- axial initial configuration of the lattice, such that the molecules are aligned with their molecular axes parallel to the laboratory frame of reference {xˆ, yˆ, zˆ}, which is parallel to

Chapter 4. Dispersion model of biaxial nematics in an external field
49
the lattice edges. That is, in the initial state, for each lattice site i:
aˆi xˆ, ˆbi yˆ, cˆi zˆ.
(3.35)
Furthermore, we put the field parallel to the zˆ axis:
_h zˆ.
(3.36)
Subsequently, the Monte Carlo step radius r, defined in (1.49), is self-consistently ad-
justed so that the average number of accepted trial moves is between 40% and 50%. As the system evolves, the acceptance may increase or lower. In particular, in the isotropic phase it can rise to as much as 60% when the radius is not adjusted. We decide to keep the radius constant during the simulation, as adjustment during simulation could lead to violation of detailed balance [112].
One Monte Carlo lattice sweep (which, generally, is called a Monte Carlo cycle in lit-
erature) proceeds by performing trial moves on N randomly chosen molecules. For a
molecule i the change in energy upon a trial rotation Ωˆ l is calculated as:
i
z=6
\

j(i)
1
2
(
\
(
\
ˆ	ˆ
ˆ	ˆ
ˆ
ˆ
∆Ei =
V (Ω , Ω ) − V (Ω , Ω ) + ∆V (Ω ) − ∆V (Ω ) ,
l
l
(3.37)
i	j
j
i
i
i
where the two particle potential and external field interaction are as defined in (3.1) and
(3.12). The trial move is accepted according to the Metropolis algorithm discussed in section 1.8.1.
As many as 100k cycles are needed for the thermalization process. For calculating av-
erages, or production, we perform from 100k to 240k cycles. As previously discussed in section 1.8, one needs to discard correlated states when calculating averages. We find that taking every tenth equilibrium configuration is a safe choice, so in the end we con- sider as many as 10k to 24k configurations when calculating thermodynamic quantities. The thermodynamic average of a general microscopic property Ai, defined for each lattice site i = 1, . . . , N , is calculated as:
( 1

M
N
M
1
M
1
\	\ Ai
=	\ A˜k ,
A =
(3.38)
N
M
k=1
i=1
k=1
k
where M is the size of the Monte Carlo statistical sample, in which
k numbers the
A˜k
elements and	is the k-th instantaneous lattice average. Furthermore, we define the

Chapter 4. Dispersion model of biaxial nematics in an external field
50
Monte Carlo fluctuation of Ai as:
 2
(
M
\

k
M
1
M
1
M
\ A˜k
k
χA = A˜2)M − A˜
˜
2
2
)M =
A −
,
(3.39)
k
where it is presented that the average ·)M is calculated as A˜
1
M
),
M Ak .
˜
)M =
k
From Monte Carlo simulations we obtain the alignment tensor Q, as defined in (3.17),
from which the director basis {l, mˆ , nˆ} is calculated by diagonalization and labeling of the respective eigenvectors according to (3.18). Order parameters q0 and q2 are then calculated from the definition (3.21).
ˆ
3.4.3.1
Specific heat and susceptibilities
To aid indication of phase transitions, we calculate the specific heat, which has an im-
portant property that it is singular at a phase transition. In the canonical ensemble the specific heat at constant volume is proportional to the fluctuation of energy:
( ∂ E) \	kB
2
2
CV =
=	( E ) − E) ).
T 2
(3.40)
∂T
V
We express CV through fluctuation of the per-particle energy:
1 z=6
 \
V (Ωˆ i, Ωˆ j ) + ∆V (Ωˆ i).
εi =
(3.41)
2
j(i)
The fluctuation of per-particle energy is calculated as in definition (3.39):

  ,
2
2
M
c = N ε˜ )
− ε˜
(3.42)
)
M
where ε˜ is the lattice average of εi. CV can be calculated from c:
kB
CV = N T 2 c.
(3.43)
For better clarity of presentation, we will use c rather than CV , because the factor 1/T 2
makes the peaks for the low-temperature transitions less visible.
It is also useful to consider susceptibilities of order parameters, which too are singular at
a phase transition. Statistical physics relates the susceptibilities to fluctuations of order parameters. Since we do not compute the instantaneous director basis for each equilib- rium state, instead of calculating fluctuations of q0 and q2, we calculate the fluctuations of scalar order parameters, given by instantaneous lattice averages of molecular uniaxial

Chapter 4. Dispersion model of biaxial nematics in an external field
51
˜
˜
T(2)
T(2)
and biaxial tensors
and	:
0
2
I
˜(2)
˜(2)
˜(2)
˜(2)
χ0 = T0 · T0 ) −	T0 · T0 )2,
(3.44)
I
˜(2)
˜(2)
˜(2)
˜(2)
χ2 = T2 · T2 ) −	T2 · T2 )2.
(3.45)
I
˜	˜
(2)	(2)
Quantities (3.44-3.45) are proportional to the susceptibilities of order parameters	T	· T	,
m	m
but we will refer to them simply as “susceptibilities of uniaxial and biaxial order param- eters”, as we do not make use of their quantitative interpretation.

Chapter 4. Dispersion model of biaxial nematics in an external field
52
3.5
Results for the Luckhurst-Romano model
As a test of our methods, we present the results recovered for the original
Luckhurst-
Romano model (3.1), i.e. when h = 0 in (3.14) for three representative values of the
parameter λ. The results are in agreement with previous research [104, 105].
The case of λ = 0.3 corresponds to prolate biaxial molecules. Results are presented in
Figs. 3.6a-c. The transition temperatures are given in Table 3.1. The phase transition sequence with lowering temperature is as follows:
In the high-temperature regime the isotropic phase (I) is present. In this phase
the order parameters q0 and q2 are zero and the invariant parameter w is undefined (because of Tr(Q2) = 0).
•
At t = tINU + a weakly first-order phase transition occurs from the isotropic (I) to
the uniaxial nematic prolate (NU +) phase. The energy fluctuation c and uniaxial
order parameter susceptibility χ0 experience sharp peaks at the transition temper- ature, while the uniaxial order parameter q0 begins to rise and w approaches 1.
•
The biaxial order parameter q2 is zero.
in mean-field.
tINU +
≈ 1.08 in Monte Carlo, tINU + ≈ 1.48
At t = tNU +NB a second-order phase transition occurs from the uniaxial nematic
prolate (NU +) to the biaxial nematic (NB ) phase. The energy fluctuation c and
the biaxial order parameter susceptibility χ2 experience peaks at the transition temperature, while the biaxial order parameter q2 begins to rise (modulus-wise),
•
whereas w begins to decrease from 1.
0.59 in mean-field.
tNU +NB
≈ 0.43 in Monte Carlo,
tNU +NB
≈
The case of λ = 0.5 corresponds to oblate biaxial molecules. Results are presented in
Fig. 3.7a-c. The phase transition sequence with lowering temperature is as follows:
As in the previous case, in the high-temperature regime the isotropic phase (I) is
present. In this phase the order parameters q0 and q2 are zero and the invariant parameter w is undefined (because of Tr(Q2) = 0).
At t = tINU − a weakly first-order phase transition occurs from the isotropic (I) to
the uniaxial nematic oblate (NU −) phase. The energy fluctuation c and uniaxial order parameter susceptibility χ0 experience sharp peaks at the transition temper-
ature, while the uniaxial order parameter q0 begins to rise (modulus-wise) and w
approaches −1. The biaxial order parameter q2 is zero.
tINU
−
≈ 1.35 in Monte
Carlo, tINU	≈ 1.85 in mean-field.
−

Chapter 4. Dispersion model of biaxial nematics in an external field
53
a
NB
b
NB
NU +
I
NU +
I
5
1
1
0.8
4
0.5
0.6
3
0.4
0
0.2
2
0
-0.5
1
-0.2
-0.4
-1
0
0.2 0.4
0.6 0.8
1
1.2
t
1.4
1.6
1.8
2
2.2
0.2 0.4
0.6 0.8
1
1.2
t
1.4 1.6
1.8	2
2.2
c
NB
NU +
I
5e-05
1e-03
4e-05
1e-03
1e-03
3e-05
8e-04
2e-05
6e-04
4e-04
1e-05
2e-04
0
0e+00
0.2 0.4
0.6 0.8
1
1.2
t
1.4
1.6
1.8
2
2.2
Figure 3.6:
Results for λ = 0.3
and h = 0.
Monte Carlo transition temperatures are
marked with vertical dashed lines, while the phases are labeled above the plot.
1. Monte Carlo (points) and mean-field (lines) uniaxial and biaxial order parameters q0 and q2 (3.21). Note how the change in mean-field q0 is abrupt, indicating the first-order character of the I − NU + transition.
2. Monte Carlo (points) and mean-field (lines) invariant parameter w (1.21) and Monte Carlo energy fluctuation c (3.42) (in green). When calculating w from Monte Carlo sim- ulations results for which Tr(Q2) < 10−3 are discarded, which happens in the isotropic phase.
3. Monte Carlo fluctuations of uniaxial (χ0) and biaxial (χ2) order parameters.
In Monte Carlo results, at temperatures directly above tINU + ≈ 1.08, minute increase in uniaxiality and biaxiality is visible (see w, q0 and q2), which is identified as a finite-size effect, often observed for such system sizes [104, 105].
The mean-field lines are composed of the high-temperature expansion result for n = 8 (see section 3.4.2.2) for t ≥ 1 and of the self-consistent result (see section 3.4.2.1) for t < 1.
q0, q2
χ0
χ2
w
c

χ0 χ2

w (mf)
w (MC)
c

q0 (MC)
q2 (MC)
q0 (mf)
q2 (mf)

Chapter 4. Dispersion model of biaxial nematics in an external field
54
At t = tNU −NB a second-order phase transition occurs from the uniaxial nematic
oblate (NU −) to the biaxial nematic (NB ) phase. The energy fluctuation c and
the biaxial order parameter susceptibility χ2 experience peaks at the transition temperature, while the biaxial order parameter q2 begins to rise, whereas w begins
to increase from −1.
tNU	B
−N
≈ 0.62 in Monte Carlo, tNU −NB ≈ 0.86 in mean-field.
1
In the self-dual case λ =	there exists one phase transition, from the isotropic (I) to
√6
the biaxial nematic (NB ) phase, which is of second order. Monte Carlo and mean-field results are presented in Fig. 3.8. The qualitative difference of the I − NB transition from the first-order I − NU and second-order NU − NB phase transitions comes from the fact
1
that for λ =	two directions of symmetry breaking (two perpendicular directors) are
√6
established simultaneously. In Monte Carlo results this leads to an apparent ambiguity of the transition temperature. In fact, the fluctuation-measuring quantities c, χ0 and χ2 are peaked at a temperature which is ∼ 18% lower than the temperature at which q0 and
q2 begin to rise (compare e.g. Figs. 3.8a and b). We infer from the results of Chiccoli
1
et al. [105] that for λ =	this mismatch is a finite-size effect and that increasing the
√6
1
system size corrects this discrepancy. In our results for λ =	we choose to interpret the
√6
temperature at which q0 and q2 are seen to increase as tINB (marked as vertical dashed lines in Fig. 3.8). From Monte Carlo tINB ≈ 1.22, while from mean-field tINB ≈ 1.6.

Chapter 4. Dispersion model of biaxial nematics in an external field
55
a
NB
b
NU −
I
NB
NU −
I
5
1
0.4
0.2
4
0.5
0
3
-0.2
0
-0.4
2
-0.6
-0.5
1
-0.8
-1
-1
0
0.2 0.4
0.6
0.8
1
1.2
t
1.4
1.6 1.8
2
2.2
0.2
0.4
0.6 0.8
1
1.2 1.4 1.6 1.8	2
t
2.2
c
NB
NU −
I
5e-05
1e-03
4e-05
1e-03
1e-03
3e-05
8e-04
2e-05
6e-04
4e-04
1e-05
2e-04
0
0e+00
0.2 0.4
0.6
0.8
1	1.2
t
1.4
1.6 1.8
2
2.2
Figure 3.7: Results for λ = 0.5
and h = 0.
Monte Carlo transition temperatures are
marked with vertical dashed lines, while the phases are labeled above the plot.
1. Monte Carlo (points) and mean-field (lines) uniaxial and biaxial order parameters q0 and q2 (3.21). Note how the change in mean-field q0 is abrupt, indicating the first-order character of the I − NU + transition.
2. Monte Carlo (points) and mean-field (lines) invariant parameter w (1.21) and Monte Carlo energy fluctuation c (3.42) (in green). When calculating w from Monte Carlo sim- ulations results for which Tr(Q2) < 10−3 are discarded, which happens in the isotropic phase.
3. Monte Carlo fluctuations of uniaxial (χ0) and biaxial (χ2) order parameters.
In Monte Carlo results, at temperatures directly above tINU	≈ 1.35, minute increase in
−
uniaxiality and biaxiality is visible (see w, q0 and q2), which is identified as a finite-size
effect, often observed for such system sizes [104, 105].
The mean-field lines are composed of the high-temperature expansion result for n = 8 (see section 3.4.2.2) for t ≥ 1 and of the self-consistent result (see section 3.4.2.1) for t < 1.
q0, q2
χ0
χ2
w
c

χ0 χ2

w (mf)
w (MC)
c

q0 (MC)
q2 (MC)
q0 (mf)
q2 (mf)

Chapter 4. Dispersion model of biaxial nematics in an external field
56
a
b
NB
I
NB
I
5
1
1
4
0.5
0.5
3
0
0
2
-0.5
-0.5
1
-1
-1
0
0.2
0.4
0.6 0.8
1
1.2
t
1.4
1.6
1.8
2
2.2
0.2 0.4 0.6 0.8
1
1.2 1.4 1.6
t
1.8
2
2.2
c
NB
I
5e-05
1e-03
4e-05
1e-03
1e-03
3e-05
8e-04
2e-05
6e-04
4e-04
1e-05
2e-04
0
0e+00
0.2
0.4
0.6 0.8
1
1.2
t
1.4
1.6
1.8
2
2.2
1
Figure 3.8: Results for λ
=	and h = 0. Monte Carlo transition temperatures are
√6
marked with vertical dashed lines, while the phases are labeled above the plot.
1. Monte Carlo (points) and mean-field (lines) uniaxial and biaxial order parameters q0 and q2 (3.21). Out of the two equivalent branches of solutions for q0 and q2, the prolate branch (q0 ≥ 0) has been chosen for presentation.
2. Monte Carlo (points) and mean-field (lines) invariant parameter w (1.21) and Monte Carlo energy fluctuation c (3.42) (in green). When calculating w from Monte Carlo sim- ulations results for which Tr(Q2) < 10−3 are discarded, which happens in the isotropic phase.
3. Monte Carlo fluctuations of uniaxial (χ0) and biaxial (χ2) order parameters.
In Monte Carlo results the transition temperature result inferred from the behavior of q0 and q2 differs from what is visible in the fluctuations of energy c and order parameters χ0 and χ2. Peaks in these quantities are much broader than for other phase transitions encountered for the Luckhurst-Romano model (3.1). It can also be told from the behav- ior of order parameter fluctuations χ0 and χ2 (c) that in a broad temperature region below the transition temperature, down to t ≈ 0.7, strong fluctuations are encountered, which affects the precision of determining q0, q2 and w.
The mean-field lines are composed of the high-temperature expansion result for n = 8 (see section 3.4.2.2) for t ≥ 1 and of the self-consistent result (see section 3.4.2.1) for t < 1.
q0, q2
χ0
χ2
w
c

χ0 χ2

w (mf)
w (MC)
c

q0 (MC)
q2 (MC)
q0 (mf)
q2 (mf)

Chapter 4. Dispersion model of biaxial nematics in an external field
57
Table 3.1: Values of the transition temperatures obtained for the Luckhurst-Romano
model (3.1).
λ

tINU (mf )
tINU (MC)
tNU NB (mf )
tNU NB (MC)
tINB (mf )
tINB (MC)
0.3

1.48

1.08

0.59

0.43

X

X

0.5

1.85

1.35

0.86

0.62

X

X

  1
√6
X

X

X

X

1.6

1.22

Chapter 4. Dispersion model of biaxial nematics in an external field
58
3.6
Studying the model with external field
We now turn to the general case, described by the model (3.14), which we investigate
using the methods described earlier.
3.6.1
Critical and tricritical points
The high-temperature expansion mean-field method is useful in finding critical and tri-
critical points, because it correctly recovers the transition order. A critical or tricritical point can be found by finding a set of conditions for the per-particle free energy (3.33), which are met at such a point exclusively. These conditions can be solved for t = tc and
∆Eh2 = ∆Eh2 to find the location of the critical or tricritical point in the (t, ∆Eh2) plane,
c
keeping λ as a constant parameter. We find that these conditions attain a particularly compact and simple form if a different decomposition of Q (rather than (3.20)), through the parameters q0 and q2 in the director basis) is adopted. Throughout this section we decompose the alignment tensor Q in a basis fixed on the direction of the field and the laboratory frame of reference {xˆ, yˆ, zˆ}:
(2)
(2)
Q = r T	({xˆ, yˆ, zˆ
) + r T	({xˆ, yˆ, zˆ
),
(3.46)
}
}
0
2
0
2
(2)
where zˆ ≡ hˆ, because we put _h zˆ. The tensors T	({xˆ, yˆ, zˆ
), m =
0, 2 are of the
m
}
form (2.8-2.9), where we substitute {eˆx ≡ xˆ, eˆy ≡ yˆ, eˆz ≡ zˆ}. The scalar parameters
r0 and r2 retain the interpretation of the uniaxial and biaxial order parameters, related through linear combinations to q0 and q2, and thus the minimization conditions for the per-particle free energy are similar:

∂
fn =
0

 ∂r0

 ∂
fn =
0

 ∂r2
(3.47)
∂2
2 fn >
0

∂r


0
∂2


f >
0.

n

2
∂r
2
fn is the expanded mean-field per-particle free energy (3.33) with Q expressed using the
decomposition (3.46):

\
\i
n
r
z
i 1
 (
i!
fn = 2 (r0 + r2 ) − t log	dΩˆ
2	2
ˆ
t−
HMF
(Ω)	,
(3.48)
−
i=0

Chapter 4. Dispersion model of biaxial nematics in an external field
59
where:
(2)
(2)
ˆ
ˆ
ˆ
H
(Ω) = −E(r T	({xˆ, yˆ, zˆ
) + r T	({xˆ, yˆ, zˆ
) · Q(Ω) − E∆Eh h
Q(Ω)	. (3.49)
}
}
MF
0
2
α β
αβ
0
2
3.6.1.1
Mean-field calculation of the critical point
We proceed to describe the critical temperature and critical field for the critical point of
the NP − NU transition upon continuous change of the parameter λ. This is achieved by first observing that at the critical point the parameter r0 has an inflection point. The inflection point at t = tc and h = hc is described by equalities:

∂t
=
0

 ∂r0

 ∂2t
=
0
(3.50)
∂r2
0

 ∂3t

=
0.
 ∂r3
0
Furthermore, we assume r2 = 0 since at non-zero field the transition is from paranematic
to nematic (NP − NU ), and there is no biaxial ordering. Subsequently:

∂t	∂t ∂f
=
= 0

 ∂r0	∂f ∂r0

 ∂2t
  ∂ ( ∂t ∂f \
=
= 0
(3.51)
∂r2
∂r
∂f ∂r
0
0
0

( ∂t ∂f \
 ∂3t
∂2

=
= 0,
 ∂r3	∂r2
∂f ∂r0
0
0
where f is the free energy per particle. In conclusion, the conditions for the critical point
can be written as:
∂2f
∂3f

∂f
 ∂r0
= 0,	= 0,	= 0
∂r2
∂r3
(3.52)
0
0
 r2 = 0.
An additional requirement is that r0 minimizes the free energy per particle f . We proceed
by numerically solving (3.52) for t and ∆Eh2, with f ≈ fn as in the expansion (3.48), in
I	I 3 l
the order n = 12 for different values of the parameter λ ∈ 0,
to obtain the critical
2
values tc and hc. Because the series in (3.48) involves λ in powers up to n, the series
1
converges faster for low λ. Therefore, a more reliable result for λ >	is obtained by
√6
I 3
first solving (3.52) for λ ∈ [0,	] and mapping the outcome to (	,	] by using the
1
1
√6
√6
2
duality transformation (3.15). The result is presented in Figs. 3.9a-c. A view of the
behavior of q0 upon passing the critical point is presented for λ = 0.3 in Fig. 3.10.

Chapter 4. Dispersion model of biaxial nematics in an external field
60
As can be seen in figures 3.9a and 3.9b, the critical field experiences an inflection point
1
in the vicinity of λ =	, where hc = 0. The presence of the critical point at zero
√6
field indicates that the I − NB transition is second-order, which is known to be the case [104, 105].
b
a
5.5
5
4.5
4
3.5
3
2.5
2
1.5
1
0.02
0.01
0
-0.01
-0.02
-0.03
-0.04
-0.05
0
0.2
0.4
0.6
λ
0.8
1
1.2
-0.05 -0.04 -0.03 -0.02 -0.01
0
0.01
0.02
∆Eh2
c
c
5.5
5
4.5
4
3.5
3
2.5
2
1.5
1
0
0.2
0.4
0.6
λ
0.8
1
1.2
Figure 3.9: Behavior of the critical point of the model (3.14). Result for n = 12 in the
mean-field expansion of the per-particle free energy (3.48).
a) ∆Eh2 versus the biaxiality parameter λ. Note that the critical field decreases when
c
1
molecular biaxiality is increased (i.e. λ =	is approached from either side). Inset :
√6
1
Zoom on the vicinity of the self-dual point λ =	(area indicated by a dashed rectangle
√6
on the main plot).
b) Critical temperature versus ∆Eh2. Points mark the critical point for special values of
c
1
λ, as labeled. Inset : Zoom on the vicinity of the self-dual point λ =	(area indicated
√6
by a dashed rectangle on the main plot).
c) Critical temperature versus the biaxiality parameter λ.
∆Eh2
tc
c
1
1
λ =
λ =
√6
√6
tc

λ = I 3	1.9
2	1.8
1.7
1.6
1.5
1.4
-0.001 0 0.001

λ = 0

λ = 1
√6

0.001
0
-0.001
0.3	0.4	0.5

λ = 1

Chapter 4. Dispersion model of biaxial nematics in an external field
61
0.3
0.25
0.2
0.15
0.1
0.05
0
1.44	1.445	1.45	1.455	1.46	1.465	1.47	1.475	1.48
t
Figure 3.10: The uniaxial order parameter r0 as defined in (3.46) passing through the
2
critical point at ∆Eh ≈ 0.007976, t ≈ 1.4566 for λ = 0.3. Note how for larger values of
c
c
h the uniaxial order increases in the NP phase above the transition temperature, which
is also increased. Above hc, the change in r0 becomes smooth, as the phase transition vanishes. Plots obtained by using the mean-field expansion (3.48) to the order n = 6. tc and hc obtained for n = 12.
3.6.1.2
Mean-field calculation of the tricritical point
For the NP − NB transition the biaxial order parameter r2 is zero in the NP phase, but
is non-zero in the NB phase. Initially discontinuous in the first-order transition, at the tricritical point both r0 and r2 experience an inflection point at temperature tc and field magnitude hc. The corresponding conditions for the mean-field free energy per particle at t = tc and h = hc are:

∂f
	= 0
∂r0
∂f
∂r2
∂2f



= 0


(3.53)
= 0

2
∂r


0
2

∂ f

= 0.
 ∂r2
2
As previously, r0 and r2 need to obey the minimum f condition. We use the expansion of the mean-field free energy per particle (3.48) to the order n = 10 and solve (3.53)
I
numerically for t and ∆Eh2 for different values of λ ∈ [0,	]. As before, we first solve
3
2
I 3
for λ ∈ [0,	] and map the result to (	,	] using the duality transformation (3.15).
1
1
√6
√6
2
r0
∆Eh2
0.0042
0.0054
0.0066
0.0078
     0.0090
0.0102
0.0114

Chapter 4. Dispersion model of biaxial nematics in an external field
62
The result is presented in Figs. 3.11a-c. Exemplary behavior of order parameters as the
tricritical point is passed is presented in figures 3.12a-b.
1
As we can see in Fig. 3.11a, the tricritical point for λ =	is present at zero field, at
√6
tc ≈ 1.6 and coincides with the critical point, thus forming the multicritical point. This further reflects the fact that the I − NB transition is second-order in the self-dual case.
b
a
5
0.1
4.5
4
0.05
3.5
3
0
2.5
2
-0.05
1.5
0
0.2
0.4
0.6
λ
0.8
1
1.2
-0.05
0
0.05
0.1
∆Eh2
c
c
5
4.5
4
3.5
3
2.5
2
1.5
0
0.2
0.4
0.6
λ
0.8
1
1.2
Figure 3.11: Behavior of the tricritical point of the model (3.14). Result for n = 10 in
the mean-field expansion of the per-particle free energy (3.48).
a) ∆Eh2 versus the biaxiality parameter λ. Note that the critical field decreases when
c
1
molecular biaxiality is increased (i.e. λ =	is approached from either side).
√6
b) Critical temperature versus ∆Eh2. Points mark the tricritical point for special values
c
of λ, as labeled.
c) Critical temperature versus the biaxiality parameter λ.
∆Eh2
tc
c
1
λ =
√6
√6
tc

λ =
λ = 0
λ = I 3
2

1
√6

λ = 1

Chapter 4. Dispersion model of biaxial nematics in an external field
63
-0.06
0.2
-0.08
0.15
-0.1
-0.12
0.1
-0.14
0.05
-0.16
0
-0.18
1.45
1.455 1.46 1.465 1.47 1.475 1.48 1.485 1.49
t
1.45 1.455 1.46 1.465
1.47 1.475 1.48 1.485
t
1.49
Figure 3.12: Behavior of r0 and r2,
2
as defined in (3.46), when
passing through the
tricritical point at ∆Eh ≈ −0.0397, t
≈ 1.4678 for λ = 0.3. Plots and values of tc and
c
c
hc obtained by using the mean-field expansion (3.48) to the order n = 10.
Uniaxial order parameter r0. Note how for larger values of h the uniaxial order
increases in the NP phase above the transition temperature, which is also increased.
Biaxial order parameter r2. Note how the biaxial order is not affected by increasing h in the NP phase above the transition temperature, which rises with increasing field magnitude.
3.6.1.3	Conclusions and comments on simulations and experiment
We have arrived at a conclusion that the critical point is not possible to locate in our
Monte Carlo setup, because determining the transition order by observing order pa- rameter discontinuities proves infeasible, as the first-order transitions are very weak. Observing the peak in the specific heat (fluctuation of energy) as the field is amplified also gives very little indication as to the position of the critical field, because a) the discontinuity in c due to latent heat at the first-order phase transition is not detectable at the considered temperature resolution, and b) there are no instances of c suddenly becoming very large at some critical field for the considered system size, which would reflect the fact that c is singular at the critical point. Moreover, the peak in c decreases in a smooth manner over a broad range of field magnitudes (see Fig. 3.14 for ∆Eh2 > 0). In conclusion, without resorting to e.g. finite-size scaling techniques, for the considered system size, Monte Carlo sample size and temperature resolution we are unable to discern the order of the transition, and therefore also to locate the critical point itself.
In our mean-field result the critical point is found for a field magnitude that is small when
compared to the temperature. However, in reality this critical field is very large and dif- ficult to achieve experimentally [113–116], which leads us to expect that the Monte Carlo result should likely reflect the reality of the experiment, i.e. that the critical field should
r0
r2
∆Eh2
-0.03
-0.032
-0.034
-0.036
-0.038
-0.04
-0.042
-0.044
-0.046
-0.048
-0.05

∆Eh2
-0.03
-0.032
-0.034
-0.036
-0.038
-0.04
-0.042
-0.044
-0.046
-0.048
-0.05

Chapter 4. Dispersion model of biaxial nematics in an external field
64
be orders of magnitude higher than mean-field theory predicts. Concerning the tricriti-
cal point, as it is predicted to exist for a higher critical field than the critical point, the critical field should be even higher in simulation, although, as is shown later, the struc- tures of the phase diagrams agree for mean-field and simulation results. Interestingly, though it is widely established that both the critical and tricritical points are present for extremely high fields for known mesogens, the behavior of both points predicted by the calculation just presented (Figures 3.9 and 3.11) is such that the critical field decreases as
1
the self dual point at λ =	is approached from either side, i.e. as molecular biaxiality
√6
is increased. Because it appears that the critical field can be made arbitrarily small for
molecules which are biaxial enough, this prediction can have experimental implications.
3.6.2
Results for λ = 0.3
For λ = 0.3 we have studied the phase diagram in the (t, ∆Eh2) plane using both the
mean-field method and Monte Carlo simulations for a range of field magnitudes h ∈
[0, 0.9] for ∆E = ±1. Such field magnitudes can be considered large in relation to e.g. the
2
mean-field result the critical point, which occurs for h ≈ 0.008 for λ = 0.3. According
c
to the discussion conducted in section 3.3.2, for ∆E = +1 we should observe uniaxiality-
promoting effects and a critical point for the NP + − NU + transition, while for ∆E = −1 biaxiality-promoting effects should be encountered, along with a tricritical point for the NP − − NB transition.
The mean-field phase diagram, displaying first order and second order transition lines, as well as critical and tricritical points, is presented in Fig. 3.13. The mean-field result confirms the above anticipations and Landau-de Gennes theory predictions completely for the isotropic-uniaxial nematic transition. In addition, we have found that the transition temperature for the NU + − NB transition is lowered with increased field magnitude for
∆E = +1, although the change is minute: a ∼ 1% decrease in tNU +NB is noted over an increase from h2 = 0 to h2 = 0.6.
For the Monte Carlo result it is most illustrative to compare the mean-field phase diagram
to the energy fluctuation landscape (c, as defined in (3.42)), pictured in Fig. 3.14. The result confirms the mean-field prediction as to the qualitative effects for both cases of
∆E = ±1. As expected, the transition temperatures are lower than in the mean-field result. However, as discussed earlier in 3.6.1.3, the critical and tricritical points cannot be precisely located based neither on the behavior of the energy fluctuation (or specific heat), nor the behavior of order parameters. Instead, we observe the following effects (as
labeled in Fig. 3.14):

Chapter 4. Dispersion model of biaxial nematics in an external field
65
A – The temperature of the
NP + − NU +
transition for ∆E = +1 rises as the
field is increased and the transition becomes smoother. However, the peak in c
does not vanish completely, but is gradually broadened and lowered. The uniaxial order parameter experiences a smooth increase with lowering temperature over the transition for higher field magnitudes (see Figs. 3.15a,c,e). No qualitative change in any of the computed quantities is noted for the mean-field prediction for
h2
≈ 0.008. In conclusion, we are unable to determine whether the critical point
c
lies in the range of the considered field magnitudes, or exists for a larger value
outside of the studied range.
B – The temperature of the NP − − NB transition for ∆E = −1 rises as the
field is increased. The peak in c is initially decreased, but stabilizes at c ≈ 4. The NP − − NB transition remains first order and the discontinuity of the uni- axial order parameter q0 is in fact increased when the field is amplified (see Figs. 3.15a,c,e). This behavior is expected to continue until the field is large enough that field-ordering of secondary molecular axes dominates over the ordering of primary molecular axes upon the NP − − NB transition, which will result in a tricritical point. However, for the considered field magnitudes we have not observed this to happen. Furthermore, no qualitative change in any of the computed quantities is
2
•
noted for the mean-field prediction for h ≈ 0.04, which leads us to the conclusion
c
that in Monte Carlo simulations the tricritical point is present for a much higher
field than the mean-field result would suggest.
C – There is no measurable change in the NU + − NB transition temperature
and the peak in c undergoes no systematic changes. We conclude that for the considered field magnitudes this transition is unaffected by increased field in Monte Carlo simulations.
•
D – For non-zero field, the NU + − NB transition begins to fade away, although
this does not occur instantly in the simulation result. The peak in c is gradually smoothed out and moves to higher temperatures with increased field. Eventually, for ∆Eh2 ≈ −0.25, it is no longer observed. The biaxial order parameter q2 ex- periences a smooth increase with lowering temperature in place of the zero-field transition (see Figs. 3.15a,c,e).
•

Chapter 4. Dispersion model of biaxial nematics in an external field
66
0.6
0.4
NB
NU +
0.2
0
NU +
0.02
0
-0.02
-0.04
-0.06
-0.2
NB
NP −
I
NP +
-0.4
NB
NP −
1.44	1.46	1.48
-0.6
0.4
0.6
0.8
1
1.2
1.4
1.6
t
Figure 3.13: Mean-field phase diagram of the
model (3.14) for λ =
0.3. Solid lines
are indicated by
represent first-order phase transitions, while second-order transitions
dashed lines. Critical and tricritical points are indicated by black filled circles in the inset. The critical point is located at (tc, ∆Eh2)cp ≈ (1.4566, 0.007976) and the tricritical point is located at (tc, ∆Eh2)tcp ≈ (1.4678, −0.0397) (result obtained by the method explained in section 3.6.1). The high-temperature transition line (NP + − NU + and NP − − NB ) was obtained with the expansion method, described in section 3.4.2.2, with n = 10 in
the expression of the approximate per-particle free energy fn (3.33). The NU + − NB
transition line was obtained with the self-consistent method, described in section 3.4.2.1.
∆Eh2

Chapter 4. Dispersion model of biaxial nematics in an external field
67
Figure 3.14: Energy fluctuation landscape for λ = 0.3 displayed as a function of ∆Eh2 and t. c is defined as in (3.42) and is proportional to specific heat. c for h = 0 is traced with a bold black line for reference. The ridges correspond to transition lines between phases, which are labeled in regular black typeface. Circled labels are explained in section 3.6.2.

Chapter 4. Dispersion model of biaxial nematics in an external field
68
a
b
NB
NU +
NP +
NB
NU +
NP +
8
1
1
7
0.8
6
0.5
0.6
5
0.4
0
4
0.2
3
0
-0.5
2
-0.2
1
-0.4
-1
0
0.2
0.4
0.6
0.8
1
1.2
1.4
1.6
1.8
0.2
0.4
0.6
0.8
1
1.2
1.4
1.6
1.8
t
t
c
d
NB
NU +
NP +
NB
NU +
NP +
8
1
1
7
0.8
6
0.5
0.6
5
0.4
0
4
0.2
3
0
-0.5
2
-0.2
1
-0.4
-1
0
0.2
0.4
0.6
0.8
1
1.2
1.4
1.6
1.8
0.2
0.4
0.6
0.8
1
1.2
1.4
1.6
1.8
t
t
e
f
NB
NU +
NP +
NB
NU +
NP +
8
1
1
7
0.8
6
0.5
0.6
5
0.4
0
4
0.2
3
0
-0.5
2
-0.2
1
-0.4
-1
0
0.2
0.4
0.6
0.8
1
1.2
1.4
1.6
1.8
0.2
0.4
0.6
0.8
1
1.2
1.4
1.6
1.8
t
t
Figure 3.15: Results for λ = 0.3 and ∆E = +1. (Caption on adjacent page).
q0, q2
q0, q2
q0, q2
w
w
w
c
c
c

w (mf)
w (MC)
c

q0 (MC)
q2 (MC)
q0 (mf)
q2 (mf)

w (mf)
w (MC)
c

q0 (MC)
q2 (MC)
q0 (mf)
q2 (mf)

w (mf)
w (MC)
c

q0 (MC)
q2 (MC)
q0 (mf)
q2 (mf)

Chapter 4. Dispersion model of biaxial nematics in an external field
69
Figure 3.15: (Left) Monte Carlo results (points) for λ = 0.3 and ∆E = +1,
compared
with mean-field results (solid lines), for h = 0.3 (a-b), h = 0.6 (c-d) and h = 0.9 (e-f ).
Monte Carlo transition temperatures are marked with vertical dashed lines, while the phases are labeled over the plot. The transition temperatures are estimated based on the peaks in the energy fluctuation c.
Left column (a,c,e): uniaxial and biaxial order parameters q0 and q2, as defined in
(3.21).
Right column (b,d,f ): invariant order parameter w, as defined in (1.21), and energy fluctuation c, as defined in (3.42).
Note how with increased field the NP + −NU + transition shifts to higher temperatures, q0
increases in the NP + phase, the transition becomes smoother and the peak in c decreases and broadens. The NU + − NB transition appears unaffected by the amplified field.

The mean-field lines are composed of the high-temperature expansion result for n = 8 (see section 3.4.2.2) for t ≥ 1.4 and of the self-consistent result (see section 3.4.2.1) for t < 1.4. The dividing temperature has been chosen this high because the mean-field free energy per particle expansion (3.33) contains ∆Eh2 to the order of n, which impairs convergence for h /= 0 in lower temperatures.

Chapter 4. Dispersion model of biaxial nematics in an external field
70
a
b
NB
NP −
NB
NP −
N l
N l
B
B
8
1
1
7
0.8
6
0.5
0.6
5
0.4
0
w (MC)
4
0.2
3
0
-0.5
2
-0.2
1
-0.4
-1
0
0.2
0.4
0.6
0.8
1
1.2
1.4
1.6
1.8
0.2
0.4
0.6
0.8
1
1.2
1.4
1.6
1.8
t
t
c
d
NB
NP −
NB
NP −
8
1
1
7
0.8
6
0.5
0.6
5
0.4
0
w (MC)
4
0.2
3
0
-0.5
2
-0.2
1
-0.4
-1
0
0.2
0.4
0.6
0.8
1
1.2
1.4
1.6
1.8
0.2
0.4
0.6
0.8
1
1.2
1.4
1.6
1.8
t
t
e
f
NB
NP −
NB
NP −
8
1
1
7
0.8
6
0.5
0.6
5
0.4
0
w (MC)
4
0.2
3
0
-0.5
2
-0.2
1
-0.4
-1
0
0.2
0.4
0.6
0.8
1
1.2
1.4
1.6
1.8
0.2
0.4
0.6
0.8
1
1.2
1.4
1.6
1.8
t
t
Figure 3.16: Results for λ = 0.3 and ∆E = −1. (Caption on adjacent page).
q0, q2
q0, q2
q0, q2
w
w
w
c
c
c

w (mf)
c

q0 (MC)
q2 (MC)
q0 (mf)
q2 (mf)

w (mf)

c

q0 (MC)
q2 (MC)
q0 (mf)
q2 (mf)

w (mf)
c

q0 (MC)
q2 (MC)
q0 (mf)
q2 (mf)

Chapter 4. Dispersion model of biaxial nematics in an external field
71
Figure 3.16: (Left) Monte Carlo results (points) for λ = 0.3 and ∆E = −1,
compared
with mean-field results (solid lines), for h = 0.3 (a-b), h = 0.6 (c-d) and h = 0.9 (e-f ).
Monte Carlo transition temperatures are marked with vertical dashed lines, while the
phases are labeled over the plot. The transition temperatures are estimated based on the peaks in the energy fluctuation c.
Left column (a,c,e): uniaxial and biaxial order parameters q0 and q2, as defined in
(3.21).
Right column (b,d,f ): invariant order parameter w, as defined in (1.21), and energy fluctuation c, as defined in (3.42).
Note how with increased field the NP − − NU − transition shifts to higher temperatures
and the peak in c initially decreases, but is retained. The reorientation of the director nˆ
from parallel to _h to perpendicular to hˆ is reflected in the change of sign in q0 and w upon the transition. The NU − − NB transition appears to exist for small values of the field
as a transition between two biaxial phases,	− NB , where	is only distinguished
N l
N l
B
B
by the fact that its biaxial ordering is field-induced and very small. This transition is
shifted towards higher temperatures, but is vanished completely as of h = 0.5 both in c
and in the behavior of q2.
The mean-field lines are composed of the high-temperature expansion result for n = 8
(see section 3.4.2.2) for t ≥ 1.4 and of the self-consistent result (see section 3.4.2.1) for t < 1.4. The dividing temperature has been chosen this high because the mean-field free energy per particle expansion (3.33) contains ∆Eh2 to the order of n, which impairs convergence for h /= 0 in lower temperatures.

Chapter 4. Dispersion model of biaxial nematics in an external field
72
3.6.3
Results for λ = 0.5
1
Because of the self-duality relation (3.15), the effects encountered for λ >	are equiv-
√6
1
alent to those present for λ <	for the opposite cases of the sign of the anisotropy
√6
of the field polarizability (∆E → −∆E) in terms of the structure of the phase diagram and symmetries of the encountered phases. However, since the duality transformation
also entails a change of the preferred molecular axis (such that the primary axis is cˆ for
λ <	and ˆb for λ >	), prolate phases (NU + and NP +) for λ <	match oblate
1
1
1
√6
√6
√6
and vice-versa. This dual symmetry is apparent
  1
phases (NU − and NP −) for λ >
√6 ,
when comparing the mean-field phase diagrams for λ = 0.3 (Fig. 3.13) and λ = 0.5 (Fig.
3.17).
According to discussion from section 3.3.2 and Landau-de Gennes theory predictions, for
∆E = +1 biaxiality-promoting effects should be observed, along with a tricritical point of the NP + − NB transition, while for ∆E = −1 one should encounter uniaxiality-promoting effects and a critical point of the NP −−NB transition. This is confirmed in the mean-field results, as presented in the mean-field phase diagram in Fig. 3.17. Additionally, as in the λ = 0.3 case, we have found that the temperature of the NU − − NB phase transition weakly decreases with increased field magnitude, i.e. we observe a ∼ 1% decrease in
2
2
tNU
over an increase from h = 0 to h = 0.4.
−N
B

Chapter 4. Dispersion model of biaxial nematics in an external field
73
0.06
0.3
NB
NP +
0.02
0
-0.02
0.2
NB
NP +
NP −
I
NU
−
0.1
1.82
1.84
1.86
0
-0.1
-0.2
NB
NU −
-0.3
0.6
0.8
1
1.2
1.4
1.6
1.8
2
t
Figure 3.17: Mean-field phase diagram of the model (3.14) for λ =
0.5. Solid blue
lines represent first-order phase transitions, while second-order transitions are indicated
by dashed blue lines. Critical and tricritical points are indicated by black filled circles in the inset. The critical point is located at (tc, ∆Eh2)cp ≈ (1.83, −0.004244) and the tricritical point is located at (tc, ∆Eh2)tcp ≈ (1.8465, 0.03164) (result obtained by the method explained in section 3.6.1). The high-temperature transition line (NP + − NU + and NP − − NB ) was obtained with the expansion method, described in section 3.4.2.2, with n = 10 in the expression of the approximate per-particle free energy fn (3.33). The NU + − NB transition line was obtained with the self-consistent method, described in section 3.4.2.1.
∆Eh2

Chapter 4. Dispersion model of biaxial nematics in an external field
74
1
3.6.4
Results for λ =
√6
For the self-dual case the biaxial nematic phase is of maximum biaxiality, i.e.	the
alignment tensor Q possesses no purely uniaxial contribution, as its eigenvalues obey
the relation	= −ωmˆ ∧ ωˆl = 0 and it is proportional to the purely biaxial tensor
ωnˆ
T(2)
({mˆ , nˆ, ˆl) =	(mˆ ⊗ mˆ − nˆ ⊗ nˆ). Any finite finite field introduces a uniaxial contri-
1
√
2
2
bution to Q and, depending on ∆E, makes one of the axes cˆ and ˆb preferred. Because Q
is traceless, a field-induced uniaxial contribution results in a decrease in the biaxial part
of Q. Therefore, the biaxial nematic phase of maximum biaxiality occurs only for h = 0.
For λ =	the molecular axes cˆ and ˆb are interchangeable, provided that simultaneously
1
√6
we change ∆E → −∆E (which follows from the duality transformation (3.15)). Such
transformation leaves the Boltzmann factor e−H/t for the Hamiltonian (3.14) invariant.
Therefore, the phase diagram for λ =	in the (t, ∆Eh2) plane is symmetric with respect
1
√6
to a reflection about the t-axis. The isotropic phase is superseded by a paranematic phase
for finite field magnitudes,
NP +
for ∆E = +1 and
NP −
for ∆E = −1. As we can see
in the mean-field phase diagram (Fig. 3.18), the I − NB transition temperature drops
rapidly upon applying even a small external field. The zero-field phase transition is second-order and the mean-field result suggests that also the finite-field phase transition is second-order as well. However, as of now, phenomenological theory of the NP − NB transition for the self-dual case is not available.
We present simulation results for small field values of ∆Eh2 = ±0.018 in Figs. 3.19-3.19.
As we can see, for non-zero field the transition to the biaxial phase is retarded towards lower temperatures (observe q2 in the aforementioned figures and compare with zero-field results in Fig. 3.8), while at t ≈ 1.2 there remains an increase in uniaxial ordering (see q0 in aforementioned figures), which qualitatively is no different from a phase transition in Monte Carlo simulations. Therefore, for the simulation result we distinguish a narrow region where the NU phase is present between NP and NB phases. Comparing the order parameter susceptibilities in Figs. 3.19c and 3.20c, we see that the NP − NU transition is accompanied by an increase in χ2 and the NU − NB transition is accompanied by an increase in χ0.
As in the result for h = 0, there are discrepancies between transition temperatures
inferred from increases in q0 and q2 and peaks in c, χ0 and χ2, attributed to a finite-size effect. As in section 3.5, we choose to determine the transition temperatures from the behavior of q0 and q2 for the self-dual case.

Chapter 4. Dispersion model of biaxial nematics in an external field
75
0.4
0.3
0.2
NB
NU +
0.1
0
I
-0.1
-0.2
NB
NU −
-0.3
-0.4
0.8
1
1.2
1.4
1.6
1.8
t
Figure 3.18: Mean-field phase diagram of the model (3.14) for λ =
1
. The second-
√6
order transition line is indicated by a blue dashed line. The multicritical point is marked by a solid filled black circle at (tc, ∆Eh2)mcp ≈ (1.6, 0) (result obtained by the method
explained in section 3.6.1). The NP −NB transition line was obtained with the expansion method, described in section 3.4.2.2, with n = 10 in the expression of the approximate per-particle free energy fn (3.33).
∆Eh2

Chapter 4. Dispersion model of biaxial nematics in an external field
76
a
b
NB
NU −
NP −
NB
NU −
NP −
5
1
1
4
0.5
0.5
3
0
0
2
-0.5
-0.5
1
-1
-1
0
0.2
0.4
0.6
0.8
1
1.2
t
1.4
1.6 1.8
2
2.2
0.2 0.4 0.6
0.8
1
1.2
t
1.4 1.6 1.8
2
2.2
c
NB
NU −
NP −
5e-05
1e-03
4e-05
1e-03
1e-03
3e-05
8e-04
2e-05
6e-04
4e-04
1e-05
2e-04
0
0e+00
0.2
0.4
0.6
0.8
1
1.2
t
1.4
1.6 1.8
2
2.2
Figure 3.19: Results for λ =	and ∆Eh2 = −0.018. Monte Carlo transition tempera-
1
√6
tures are marked with vertical dashed lines, while the phases are labeled above the plot.
1. Monte Carlo (points) and mean-field (lines) uniaxial and biaxial order parameters q0 and q2 (3.21). Out of the two equivalent branches of solutions for q0 and q2, the prolate branch (q0 ≥ 0) has been chosen for presentation.
2. Monte Carlo (points) and mean-field (lines) invariant parameter w (1.21) and Monte Carlo energy fluctuation c (3.42) (in green). When calculating w from Monte Carlo sim- ulations results for which Tr(Q2) < 10−3 are discarded, which happens in the isotropic phase and in the NP + phase when the field-induced ordering is very small.
3. Monte Carlo fluctuations of uniaxial (χ0) and biaxial (χ2) order parameters.
Compare the presented results with Fig. 3.8 to note that the transition to the NB phase
shifts considerably towards lower temperatures (tNP
≈ 0.98) when even a small field
−N
B
is applied. In Monte Carlo results we also distinguish an intermediate nematic uniaxial
(NU −) phase, characterized by substantially larger uniaxial ordering than in the field-
induced paranematic phase (NP −), where it is below measurement precision (for the considered field magnitude).
The mean-field lines are composed of the high-temperature expansion result for n = 8
(see section 3.4.2.2) for t ≥ 1 and of the self-consistent result (see section 3.4.2.1) for
t < 1.
q0, q2
χ0
χ2
w
c

χ0 χ2

w (mf)
w (MC)
c

q0 (MC)
q2 (MC)
q0 (mf)
q2 (mf)

Chapter 4. Dispersion model of biaxial nematics in an external field
77
a
b
NB
NU +
NP +
NB
NU +
NP +
5
1
1
4
0.5
0.5
3
0
0
2
-0.5
-0.5
1
-1
-1
0
0.2 0.4
0.6
0.8
1
1.2
t
1.4
1.6 1.8
2
2.2
0.2
0.4 0.6
0.8
1
1.2
t
1.4 1.6 1.8
2
2.2
c
NB
NU +
NP +
5e-05
1e-03
4e-05
1e-03
1e-03
3e-05
8e-04
2e-05
6e-04
4e-04
1e-05
2e-04
0
0e+00
0.2
0.4
0.6
0.8
1	1.2
t
1.4
1.6 1.8
2
2.2
1
and ∆Eh2 = 0.018.
Figure 3.20: Results for λ =
Monte Carlo transition temperatures
√6
are marked with vertical dashed lines, while the phases are labeled above the plot.
1. Monte Carlo (points) and mean-field (lines) uniaxial and biaxial order parameters q0 and q2 (3.21). Out of the two equivalent branches of solutions for q0 and q2, the prolate branch (q0 ≥ 0) has been chosen for presentation.
2. Monte Carlo (points) and mean-field (lines) invariant parameter w (1.21) and Monte Carlo energy fluctuation c (3.42) (in green). When calculating w from Monte Carlo sim- ulations results for which Tr(Q2) < 10−3 are discarded, which happens in the isotropic phase and in the NP + phase when the field-induced ordering is very small.
3. Monte Carlo fluctuations of uniaxial (χ0) and biaxial (χ2) order parameters.
Compare the presented results with Fig. 3.8 to note that the transition to the NB phase
shifts considerably towards lower temperatures (tNP +NB ≈ 0.98) when even a small field is applied. In Monte Carlo results we also distinguish an intermediate nematic uniaxial (NU +) phase, characterized by substantially larger uniaxial ordering than in the field- induced paranematic phase (NP +), where it is below measurement precision (for the considered field magnitude).
The mean-field lines are composed of the high-temperature expansion result for n = 8
(see section 3.4.2.2) for t ≥ 1 and of the self-consistent result (see section 3.4.2.1) for
t < 1.
q0, q2
χ0
χ2
w
c

χ0 χ2

w (mf)
w (MC)
c

q0 (MC)
q2 (MC)
q0 (mf)
q2 (mf)

Chapter 4. Dispersion model of biaxial nematics in an external field
78
3.7
Summary
We have explored the effects of a general vector field in the l = 2 dispersion model of
biaxial liquid crystals (3.14). Three distinct classes of phase diagrams in the (t, ∆Eh2)- plane have been identified for the prolate, oblate and self-dual case. Examples have been studied in detail with mean-field methods for the prolate case of λ = 0.3 (Fig. 3.13), for the oblate case of λ = 0.5 (Fig. 3.17) and for the self-dual case (Fig. 3.18). The behavior of the critical and tricritical points has been studied for the entire spectrum of the biaxiality parameter λ ∈ [0, 2 ], presented in Fig. 3.9 and Fig. 3.11.
I 3
3.7.1	Phase diagrams and order parameters
3.7.1.1	λ = 0.3
For the prolate case of λ = 0.3, mean-field calculations show an increase in the I − NU +
phase transition temperature with increased field, while the isotropic phase I is replaced by the field-induced paranematic prolate phase NP + for positive sign of the anisotropy of the field polarizability ∆E = +1 and by the paranematic oblate phase NP − for ∆E =
−1. The
NP + − NU +
phase transition, occurring for ∆E = +1 is first-order, until it is
terminated at a critical point for critical field hc ≈ 0.008. For ∆E = −1, field-induced
biaxiality emerges in the zero-field nematic uniaxial prolate phase NU +. The NP − − NB transition is initially first-order, but changes to second-order as the critical field hc ≈ 0.04 is passed. The NU + − NB transition, occurring for ∆E = +1 is largely unaffected by the increased field, however we do note a ∼ 1% decrease in the transition temperature, when the field is increased from h2 = 0 to h2 = 0.4. For ∆E = −1 said transition disappears, as both phases are now biaxial.
By Monte Carlo simulation we have obtained the energy fluctuation landscape as a
function of t and ∆Eh2 for the case of λ = 0.3 for h ∈ [0, 0.9] and ∆E = ±1, presented in Fig. 3.14. The result shows qualitative agreement with mean-field predictions, presented in Fig. 3.13, as to the structure of the phase diagram and the phases encountered. However, the methods employed did not allow for precisely determining the position of the critical point, which appears to lie for a field magnitude much higher than mean-field theory predicts. The tricritical point is believed to exist for a critical field well outside the considered range of field magnitudes.
Order parameters from both Monte Carlo simulations and mean-field calculations have
been compared in Figs. 3.15-3.16. The discussed effects are identified by the behavior of order parameters q0 and q2 (3.21) and the invariant order parameter w (1.21). Namely,

Chapter 4. Dispersion model of biaxial nematics in an external field
79
in paranematic phases the uniaxial order parameter q0 is non-zero and increases as the
field is amplified, while its sign identifies whether the phase is of the prolate or oblate
variety (q0 > 0 for
NP +
and q0 < 0 for NP −). For ∆E = +1 the gradual smoothing
of the
NP + − NU +
phase transition is evidenced by the smoothing of q0 and the peak
in the energy fluctuation c, defined in (3.42). For ∆E = −1, q0 undergoes a change
of sign from q0 < 0 to q0 > 0 upon the NP − − NB transition, which reflects the fact
that in the
NP −
phase the field orients the director nˆ parallel to the field, while upon
the phase transition nˆ is aligned in perpendicular to the field. As the field is amplified,
the biaxial ordering in the field-induced NB phase rises, identified by rising (modulus- wise) q2. The zero-field NU + − NB phase transition vanishes instantly in the mean-field result for h /= 0, however in Monte Carlo results there briefly exists a transition between
two biaxial phases:
N l
— NB , where
N l
is only distinguished by the fact that it is
B
B
field-induced and has very small biaxial ordering. As the field is increased, this phase
transition moves towards higher temperatures and is vanished as of h = 0.5.
3.7.1.2
λ = 0.5
For the oblate case the dual symmetry of the model (3.14), defined by (3.15), is manifested
when one compares the mean-field phase diagram for λ = 0.5 (Fig. 3.17) with the phase diagram for the prolate case for λ = 0.3 (Fig. 3.13). Namely, the phase diagrams are ones mirror images (qualitatively), with the NP + and NU + phases exchanged with NP − and
NU −
phases respectively. To avoid redundancy, the discussion of the effects is omitted.
1
3.7.1.3
λ =
√6
1
The self-dual case, λ =	, for h = 0 contains a biaxial phase which is of maximum
√6
biaxiality, i.e. the alignment tensor Q does not contain a purely uniaxial contribution. Field-induced uniaxiality for h /= 0 causes a decrease in biaxiality and lowers the I − NB transition temperature rapidly, even for small fields. The high temperature phase has field-induced uniaxial ordering and is therefore a paranematic phase, NP + and NP − for
∆E = +1 and ∆E = −1 respectively. We have obtained a mean-field phase diagram for
1
λ =	, presented in Fig. 3.18. Because of dual symmetry, defined in (3.15), the phase
√6
diagram is symmetric with respect to a reflection about the t-axis. There is only one transition line in the diagram, the NP − NB phase transition line, with a multicritical point at (tc, hc) ≈ (1.6, 0), where six phases: I, NU +, NU −, NP +, NP −, NB meet (when
considering both (t, ∆Eh2) and (λ, t) phase diagrams).
1
The effects of an external field on the behavior of order parameters in the case of λ =
√6
are presented in Fig. 3.19-3.20, where both mean-field and Monte Carlo simulation results

Chapter 4. Dispersion model of biaxial nematics in an external field
80
are presented. In both cases of ∆E = ±0.018 the Monte Carlo transition to the NB phase
is retarded to tNP NB ≈ 0.98 with respect to the zero-field transition at tINB ≈ 1.22, as presented in Fig. 3.8. In Monte Carlo results we are compelled to treat the increase in q0 at t ≈ 1.2 as a separate phase transition, therefore there is a region where in simulations an intermediate uniaxial nematic phase exists, NU + for ∆E = +1 and NU − for ∆E = −1, between NP and NB phases.
3.7.1.4
Mean-field study of critical and tricritical points
The mean-field high-temperature expansion method has been used for a detailed study
of the behavior of critical and tricritical points, depending on the parameter λ ∈ [0, 2 ]. To this end conditions for the critical (3.52) and tricritical (3.53) points have been found and solved numerically for the critical and tricritical field and temperature, with the result presented in Fig. 3.9 and Fig. 3.11. We have taken advantage of the duality transformation (3.15) to improve the convergence of the mean-field expansion of the per-
I 3
I 3
particle free energy (3.48) by transforming the result for λ ∈ [0,	] to λ ∈ (	,	].
1
1
√6
√6
2
The result confirms that the critical and tricritical points are located for ∆Eh2 > 0 for
1
1
1
λ <	and ∆Eh2 < 0 for λ >	respectively and travel towards ∆Eh2 = 0 as λ =
√6
√6
√6
is approached from either side, that is, the critical field is seen to decrease as molecular
1
biaxiality is increased. At λ =	both points coincide, thus forming the multicritical
√6
point, at which, in the “super” phase-diagram in the parameter space of (t, λ, ∆Eh2), six
  1
phases meet: I, NU +, NU −, NP +, NP − and NB . As λ is increased over
√6 ,
the critical
and tricritical points emerge at opposite sides of the ∆Eh2 = 0 line, for ∆Eh2 < 0 and
∆Eh2 > 0 respectively, which reflects the dual symmetry of the model (3.14).

Chapter 4
Tetrahedratic order and chiral
symmetry breaking in a dispersion model of liquid crystals
4.1
Introduction
Developments of the last two decades show that bent-shaped mesogens (bent-core com-
pounds, certain ferrocene mesogens and flexible dimers) exhibit many fascinating struc- tures [36, 37, 41, 44, 117]. Of particular interest is the possible existence of biaxial
order [27, 29, 30, 32, 88], spontaneous chirality and formation of chiral supramolecu- lar structures and helices [38–40, 43], the twist-bend nematic phase [45–50], as well as tetrahedratic order [51, 52, 54, 55]. In the present chapter we explore a minimal-coupling dispersion model [1, 118] which exhibits biaxiality, tetrahedratic order and chiral symme- try breaking and can be used to describe behavior in certain systems of supramolecular bent mesogen complexes. The results presented in this chapter have been published in
[119].
The minimal-coupling model is devised upon the arguments of Lubensky and Radzi-
hovsky [51], who give thorough group-theoretical classification of tensorial order param- eters and phase sequences which can emerge in bent-core systems. Their finding shows that to account for chiral ordering, at the microscopic level interactions should involve couplings of biaxial quadrupolar (second-rank) and tetrahedratic octupolar (third-rank) tensors, as well as a vector to account for the static (steric or electric) dipole. The inclusion of tetrahedratic tensors is also shown to lead to e.g. ambidextrous chirality [55, 120], i.e. twisted domains of opposite handedness. A study involving a purely tetra- hedratic interaction was notably performed by Fel [121], predicting a second-order phase
81

Chapter 5. Tetrahedratic order and chiral symmetry breaking in a dispersion model of
liquid crystals
82
transition from isotropic to a nematic tetrahedratic phase. A Monte Carlo study was
performed by Romano [122], in which case a weakly first-order transition was found.
4.2
Dispersion model with tetrahedratic coupling (infinite
pitch limit)
The model proposed in [1] is designed considering biaxial and tetrahedratic multipolar
couplings in the pair dispersion potential:
I
l
(3)
(3)
ˆ	ˆ
ˆ
ˆ
ˆ
ˆ
V (Ω , Ω ) = −E Q(Ω ) · Q(Ω ) + τ T	(Ω ) · T	(Ω ) .
(4.1)
i	j
i
j
i
j
2
2
The full Hamiltonian is obtained by performing a sum of terms (4.1) over nearest neigh-
bors on a simple cubic lattice of N particles with periodic boundary conditions:
N
1
H =	\ V (Ωˆ i, Ωˆ j ).
(4.2)
2
(i,j)
This model corresponds to the general model (2.11) for the case when all parameters
aside from λ, E and τ are zero. In our discussion we will assume that the model is studied with respect to the dimensionless temperature t = kBT/E.
As in the previous cases, the dot products in (4.1) are understood as full contractions
over Cartesian indices. The quadrupolar tensor Q(Ωˆ i) is defined in (3.2). We recognize that when τ = 0, the model reduces to the l = 2 model of biaxial nematics (3.1), as studied previously [64, 104, 105] and in Chapter 3, while the term proportional to Eτ is related to the model due to Fel [121]. While the two terms by themselves are rotationally invariant, a potential like (4.1) needs to establish a relation between the orientation of the
axes of T(2) and T(3). In (4.1), the quadrupolar part remains identical to (3.1), while in
m
2
the tetrahedratic term the tensor T(3)(Ωˆ i) is the l = 3 irreducible spherical tensor (2.10),
2
symmetrized with respect to the full tetrahedratic group Td with the assumption that the tetrahedratic twofold symmetry axes coincide with the D2h twofold symmetry axes of the quadrupolar tensor. The potential (4.1) does not contain cross-coupling terms between quadrupolar and octupolar tensors, but it can be shown that this precise arrangement of axes realizes the minimum of the lowest-order cross-coupling terms, which turns out
to be zero.
The choice of symmetry axes has a physical interpretation. The relative alignment of
the quadrupolar and tetrahedratic tensors corresponds to a ground state configuration of two bent molecules, in which they align in an embrace-locked fashion, as presented

try breaking in a dispersion mode
Chapter 5. Tetrahedratic order and chiral symme
l of
liquid crystals
83
D WYDRO
 PHYSICAL REVIEW E 79, 040701(R)(2009)
)(Oi)· Tˆ ( )(Oj)= D
L
(L)
are linear combi-
m'
mm
'
tation matrices [18].
n be interpreted within point dispersion
J
ˆ
ˆ
(2)
(2)
n. The quadrupolar tensor T	+ 2AT
0
2
to the anisotropic part of the dielectric
ˆ
(3)
of a molecule, while T	is the
2
onent of the third-order polarizability
rameters {E , A, T} are related to the mo-
equencies.
FIG. 1. (Color online) Ground-state configurations of opposite
he model have already been studied. For
Figure 4.1: Two ground state configurations for bent molecules, forming* non-polar chiral
chirality (0 < o < TI 2) for a pair of bent-core molecules in NT
l in Eq. (1) reduces to the well-known
opfhaospe;ptohseitceoncfihgiurraaltiiotyn.s foTr h0e<mo <olTIec2ulcaarnnboat sbees b{roaˆu,gˆbh,tcˆ}intoand {aˆm, ˆbm, cˆm}
wohl-Lasher [19] potentipaal,irwchoicmhpdleex- es
ram with isotropic and unciaoxrriaelspneomndatitco thecooinrcdiidneancreybaynadprroepfleercrtoetadtiobna.s(eaˆsm ,obˆfmo, pcˆmp)oasrietemihrraonr dimedagneessos.f (Reprinted with
a first-order phase transitpioenrm. Siescsioonnd fisrom [(1aˆ ],,bˆ ,Qccˆ)2. 009 by the American Physical Society.)
and T = 0. Potential (1) then reduces to
by Luckhurst et al. [20], which was
from F. The methods are the MF approximation and the
[21]. TinheFmigo.de4l .1de. - As Mweetrsoepeo, litsheMcComsipmleuxlaetsioansrewniothn-apoclraurc,iabl esctaeupsebetinhge tdhiepoles (parallel to
by Biscarini et al.
ram with uniaxial
nemattihc eanbdisebciatoxiralof thiedeonptiefinciantgionanogflet)hecaonrdceerl opuarta,mwehteircsh. jTuhsetifiideesnttihfiecaotimonissision of a vector in
ected by the second-order phase transi-
achieved by expanding the one-particle distribution function
(4.1), and exhibit conformational chirality as the relative twist angle δ ∈ [0, π) is varied.
lude: a prolate uniaxial (N ) phase, an
P(p , O) in a series of symmetry adapted real D functions,
U+
π ,
) phase, a biaxial (NB)
Fphoarsea,nyanδd /=an 0 and δ /=	the conformation has D2 non-polar chiral symmetry and is
2
A self-dual point for which A=1 J6
2L +1
L
(L)	(L)
available in two states, each obtained by a reflection about the origin of the other (left
P(p,O) =
p D	p D	(O),	(3)
s
s
hase in which the molecules are of dis-
8TI2
mm	mm
'
'
(A< 1 J6) from a phaseanind wrhigichht
tphoertions of Fig. 4.1). TL,mh,em's,special cases of δ = 0 and δ =	correspond to
π
2
orted oblate form (A> 1 J6). Bates and
with X = 1
2 Lp=±1fX(p , O)P(p , O)dO, ps =(1, p), and
non-chiral biaxial D2h and full tetrahedratic Td symmetry, respectively. It is speculated
a simple relation between E, A and the
L f
that forming of such complexes as in Fig. 4.1 is responsible for homogeneous chirality
ent-core molecules based on segmental
1
2
dOp D(L)(O)p D(L') (O)
ons [22].
s
mn	s'
m'n'
and tetrahedratic order [1].
p±1
rm proportional to ET is retained in Eq.
2
del corresponds to a purely tetrahedratic
8TI
anAdltshtuoduigedh tvhiae discussion just cited is v
alid for the type of construction pictured in Fig.
o	o	o	o	.
=
(4)
troduced by Fel [23]
LL mm nn ss
'	'	'	'
(2L + 1)
Monte Carlo (MC) simu4la.t1i,ontshebytwRoo-states of opposite chirality, parametrized by a binary microscopic variable
For the interaction of Eq. (1), the allowed symmetry re-
model, MF theory predicts a second-
pi (2.15), may be more general. For instance, flexible dimers and bent-core molecules
duction is shown in Fig. 2 along with the primary order
n from I to T phase and MC simulations
-order transition from I toarTe. terminated with flexible alkyl chains at both ends and have an unlimited number of
upolar and octupolar intercaocntifoonrsmiantEioqn.s, most of which are cIhsoirtraolpaicn: dI {oOn(3a)v}erage can be divided into two classes
es of which the most notable one is the
g of chiral symmetry. Sucohf acosnyfmormmetartyions of opposite chirality, parametrized by pi. To both of these classes there
(2)
..:
manifested in the ground-smtaateypcroorpreerstipeos nd many confor
(3)
..:
00
mational states of the molecules, but we assume that apart
22
Eq. (1). Indeed, to be consistent with Eq.
Uniaxial:
of ftrwoombtehnet-icrocrheirality they do not modify the quadruTpeotrlaahreidnrtaetirca: ction in an essential way.
lecular configurations
NU { Doo h }
T { Td }
l phase must belong to one of two con-
Therefore the considered model (4.1) is not limited to a picture like in Fig. 4.1.
(2)
(3)
ite chirality (0 < o < TI 2), as shown in
..:22
..:22
..:(2)
00
global O(3) invariance of H, the two
In (4.1), chirality manifests itself when reflections of the molecular basis	= {aˆ, ˆb, cˆ}
Ωˆ
Biaxial:
fferent chirality are the source of two
Nematic
, which are present with etqhuaatl pdroobnaobtil-preserve handeNdBn{eDss2 ha}re considered.
UTnetdrearhesdurcahtic:reflection the quadrupolar
onfiguration space. When T =0 (o =0) or
tensor Q(Ω) is left invariant, while the octupolar teNnTs{oDr 2Td (}3)(Ωˆ ) changes sign. Although
ˆ
..:(3)
22
(2)
2
molecular configurations are nonchiral
..:22
by a 90◦ rotation about one of the twofold axes leaves T(3)(Ωˆ )
nto coincidence by a rotatiaonr.eIflnepcatritoincu-followed
2
the two chiral states (Fig. 4.2) are
ons produce NU, NB, T, ainndvaNrTiapnhta, siets.is
not a symmetry of Q(Ωˆ ). Thus,
Chiral: NT * { D2 }
iral configurations to be equivalent, the
by the parity of the molecular basis p = aˆ · (ˆb × cˆ) = ±1, which can be
of the kth molecule shoduilsdtiningvuoilsvheeda
FIG. 2. (Color online) A flowchart of phase transitions between
ilinqduiedp-cernydstealntp,hadseisscfroertme odleecgurleese inotferfarcetiendgotmhr.ougThhpearier fpoortee,n-from
y pk = aˆ k · (bˆ k cˆk) = ± 1, tsheepreabryatreedfleacts- an
now on we
ry. Consequently, the free energy for thˆe
tiaˆl, Eq. (1). Primary order parameters, which become nonzero at
ˆ
is rgeinvaemn eby{aˆJ3, bF, cˆ} ≡ Ωl and imply that the generalized coordinates for molecule i are Ωi ≡
f N such molecules
the transitions, their symmetry groups and abbreviated notation for the structures are indicated. In addition, sketched are one-particle spherical distribution functions P �const+ aY20 + b(Y22 + Y2−2)
+ ci(Y32 − Y3−2) illustrating symmetries considered.
N
( 1
Ilk=1
L
fdO )exp[−J3H], and J3
p =±1	k
2
k
rse temperature.
o methods to determine phase diagrams
040701-2

RAPID COMMUNICATIONS

Chapter 5. Tetrahedratic order and chiral symmetry breaking in a dispersion model of
liquid crystals
84
a
b
Figure 4.2: Two molecular states of (4.1) of opposite chirality, a) p = 1 and b) p =
T(3)Ωˆ
The quadrupolar tensor Q(Ωˆ ) is visualized in blue; the octupolar tensor
−1.
is
2
(3)
ˆ
ˆ
visualized in orange. Surfaces obtained as r = exp(Q(Ω) · uˆ ⊗ uˆ) and r = exp(T	(Ω) ·
2
uˆ ⊗ uˆ ⊗ uˆ), where uˆ is a unit vector expressed in polar coordinates.
{pi, (aˆi, ˆbi, cˆi)}. Being an independent degree of freedom, parity needs to be included in
the trace in the definition of the canonical ensemble average (1.3), therefore it is assumed
[
dΩˆ l . Taking this degree of freedom into account means that we
≡ ),pi=±1	i
that	Tr
{Ωˆ i,pi}
allow the molecules to have two different conformations of opposite chirality.
A parity flip amounts to inverting one or more of the molecular axes or, equivalently,
changing the sign of T(3)(Ωˆ ) (while Q(Ωˆ ) remains invariant). Therefore, we can write
2
the tetrahedratic term of (4.1):
(3)
(3)
(3)
(3)
ˆ	ˆ
ˆ
ˆ
ˆ
ˆ
V (Ω , Ω ) = −Eτ T	(Ω ) · T	(Ω ) = −Eτ T	({
p , (aˆ , b , cˆ )}) · T	({
p , (aˆ , b , cˆ )}
) =
T	i	j
i
j
i
i	i	i
j
j	j	j
2
2
2
2

= −Eτpipj T2 ({aˆ , b , cˆ }) · T	({aˆj , ˆbj , cˆj }).
(3)
ˆ
(3)
i	i	i
2
(4.3)
Here pi, pj = ±1 are parities at the lattice sites i and j. We observe that the tetrahedratic
term is equal to the scalar product of tetrahedratic tensors in the canonical (right- handed) molecular bases, multiplied by the parities pipj . The minimum of (4.1) with respect to the separated degrees of freedom is such that not only all molecular axes of molecules i and j are in parallel, but also that pi = pj . Thus, the ground state favors homogeneous chirality. However, as we discuss in Chapter 5, the considered symmetries
allow for constructing an antisymmetric tensor out of T(3)(Ωˆ ), T(2)(Ωˆ ) and T(2)(Ωˆ ), and
2
0
2
therefore the ground state is unstable with respect to spontaneous formation of helical
twists. Thus, the discussion of this chapter is to be treated as the infinite pitch limit of the proper minimal coupling model.
4.2.1
Order parameters
The model (4.1) leads to a multitude of phases of non-standard symmetries. As in the
case of the l = 2 model of biaxial nematics (3.1), which is responsible for uniaxial and

Chapter 5. Tetrahedratic order and chiral symmetry breaking in a dispersion model of
liquid crystals
85
biaxial nematic ordering, the appropriate order parameters for monitoring D∞h and D2h
symmetries are the uniaxial and biaxial order parameters q0 and q2, as defined in (3.21),
while the definition of the alignment tensor Q (3.17) holds.
Monitoring of tetrahedratic order is performed through the ensemble average of the Td-
symmetry-adapted function:
∆(3)
= T2 ({l, mˆ , nˆ}) · T2 (Ωˆ ),
(3)
ˆ
(3)
(4.4)
22
ˆ
ˆ
ˆ
ˆ
where we have substituted Ω ≡ {
l, mˆ , nˆ} and Ω
≡ Ω in the definition (2.6) and applied
1
2
(3)
ˆ
the ensemble average to both sides, assuming that T	({l, mˆ , nˆ}) is constant. Further-
2
(3)
more, calculating
∆22
can be done without determining the director basis at all (thus
limiting the error due to diagonalization), by observing that:
T(3)
(3)
(Ω) · T	(Ωˆ ) =
ˆ
2
2
   2
(
(3)\
(4.5)
\

m=0,±1,±2,±3
T(3)
(3)
ˆ
(3)
ˆ
(3)
ˆ
) · T	(Ωˆ ) =	∆
=
(Ω) · T	({l, mˆ , nˆ}
) ⊗ T	({l, mˆ , nˆ}
,
2
m
m
2
22
where we have inserted the Td-symmetrized identity operator for the l = 3 subspace of
angular momentum (2.7) and observed the orthogonality relations for irreducible tensors.
Thus, we use the identity:

I

∆(3)
(3)
(3)
ˆ
) · T	(Ωˆ )
=	T2 (Ω
(4.6)
22
2
to calculate ∆(3).
22
Phase chirality is measured by the ensemble average of the molecular parity:
p = aˆi · (ˆbi × cˆi).
(4.7)
It is shown that the leading mean-field contribution to p reads [1]:
 √2
(3)
2
3
p ≈ 210t4 τλ(−3 + 2λ )∆22 q2 ,
(4.8)
which indicates that macroscopic chirality is induced by non-zero tetrahedratic
coupled with biaxiality. (p = 0 in uniaxial states.)
order
4.2.2
Phases of model (4.1)
Apart from the phases known to exist for the quadrupolar model (3.1), which are the
uniaxial nematic NU and biaxial nematic NB phases, there are additional phases in (4.1),

Chapter 5. Tetrahedratic order and chiral symmetry breaking in a dispersion model of
liquid crystals
86
in which tetrahedratic order is non-zero:
The tetrahedratic phase T , characterized by global symmetry of the full tetrahe-
•
dratic group Td (Fig. 4.3a). This phase is identified by non-zero ∆(3) and vanishing
22
uniaxial and biaxial order parameters. The molecular arrangement which produces this phase is achieved when all of the molecular tetrahedratic threefold symmetry axes align in parallel. The relative arrangements of molecular bases which satisfy this condition are realized randomly and on average none of the twofold axes of
the quadrupolar tensors are distinguished.
The nematic tetrahedratic phase NT , characterized by global dihedral symmetry
described by the point group D2d (Fig. 4.3b). An example of an object which bears the D2d symmetry is a tetrahedron stretched or compressed along one of its twofold axes. NT differs from T in the respect that also the uniaxial order parameters
•
∆(2)
q0 and
are non-zero. This phase is also referred to as “uniaxially deformed
02
tetrahedratic phase”. Much like NU , NT comes in two varieties, depending on the
type of the deformation: prolate
NT +
(stretched) and oblate
NT −
(compressed).
The molecular arrangement which produces this phase is achieved when all of the
molecular tetrahedratic threefold symmetry axes align in parallel, with an addition that the uniaxial symmetry axes of the quadrupolar part are also parallel. The relative arrangements of molecular bases which satisfy this condition are realized randomly and none of the secondary twofold axes of the quadrupolar tensors are distinguished.
The chiral nematic tetrahedratic phase N ∗ , characterized by global dihedral sym-
•
T
metry of the D2 point group (Fig. 4.3c). An example of an object which bears this symmetry is a tetrahedron which is twisted along one of its twofold axes. In
this phase, apart from non-zero tetrahedratic and uniaxial order parameters, also
∆(2)
the biaxial order parameters q2 and
are non-zero and, consequently, also is
20
the macroscopic parity p. This is the lowest-symmetry phase that is available in
the model (4.1). The molecular arrangement which produces this phase is achieved when all of the corresponding molecular basis vectors are in parallel, i.e. aˆi aˆj ,
ˆbi ˆbj , cˆi cˆj , while pi = pj .

Chapter 5. Tetrahedratic order and chiral symmetry breaking in a dispersion model of
liquid crystals
87
a
b
c
Figure 4.3: Simplified representations of the single-particle distribution functions for the
nonstandard phases exhibited by (4.1): a) T , b) NT , c) N ∗ .
T
All the phase transitions, except for those where the uniaxial parameter assumes a non-
zero value, i.e. I − NT (isotropic to nematic tetrahedratic), T − NT (tetrahedratic to nematic tetrahedratic) and I − NU (isotropic to nematic uniaxial), are second-order. The phase diagram in the (λ, t) plane depends greatly upon the parameter τ , which has several special values, with respect to which four classes are distinguished [1, 118, 119]. It has been found via bifurcation analysis that there exists a highly-symmetric value
28 ,
1
of τ =	for which at the biaxial self-dual point λ =	and temperature t = 8/5 a
√6
15
multicritical Landau point is predicted, where six phases, I, NU −, T , NT +, NT − and N ∗ ,
T
28
28 .
meet. There are two phase diagram classes for τ <	and two for τ >	For τ � 1.54,
15
15
the high-temperature regime is dominated by nematic phases (NU , NT and NB ) and
28
there is no purely tetrahedratic phase T . For 1.54 � τ <	the T phase is found and
15
28
a first-order T − NT + transition is present. For	> τ � 6.16 there is no stable NB
15
phase, while the remaining nematic uniaxial phase is NU −; the I − NU − transition line
meets with the NU − − NT −, I − T and T − NT − transition lines at a bicritical point. The last class of diagrams for τ � 6.16 exhibits a direct I − T second-order transition
and no purely nematic phases. In all phase diagram classes the temperature of the N ∗
T
1
phase is highest at the biaxial self-dual point λ =	.
√6
4.2.3
Scope of presented research
The results presented in subsequent sections pertain to the nematic-dominated phase
diagram class for τ � 1.54, i.e. τ = 1 in our case, and the phase diagram containing the
multicritical point for τ = 28 , presented in Fig. 4.4b. For these two values Monte Carlo
15
temperature scans are performed for two generic values of the biaxiality parameter λ:
1
0.3 and 0.5, and the biaxial self-dual value λ =	. In the case of τ = 1, the results
√6
supplement the phase diagram (Fig. 4.4a), obtained in [1], with temperature scans.
Throughout the following sections we assume E = 1.

sion model of
88
of
Chapter 5. Tetrahedratic order and chiral symmetry breaking in a disper
TROJANOWSKI, PAliJqAu˛Kid, LcOrNyGstAa,lsAND WYDRO
PHYSICAL REVIEW E 86, 011704 (2012)
CHIRAL SYMMETRY BREAKING IN BENT-CORE LIQUID 
PHYSICAL REVIEW E 79, 040701(R) (2009)
III. MEAN-FIELD RESULTS
phas6e diagrams for T = 1 and for T = 9 are shown in Figs. 3
5
and 4, respectively. Figure 3 shows a phase diagram in which the high-temperature regionI is dominated by the nematic
In mean-field
we average the interaction energy to
•
I
•
NB
phases. Figure 4 shows a phase diagram in which occurs a direct I-T phase transition. Phase diagrams for intermediate
•
•
•
• • • •
3
• •
NU-
•
•
•
N	Ji.
values
T can partly be deduced by extrapolation. One of
• • ••••••• •
them is of particular interest. Namely, for T = 28 six phases: I,
•
•
1
•
15
N
N
*
NU+
•
•
•
T, NT+, NT, NT−, and NU− meet at a single multicritical Lan-
•

•
•
P (p ,Q ,p ,Q ,
.. . ,p ,Q
)
•
P (p ,Q ) ≡
P (i),
•
=
••
T
N	1	1 2	2••	•
N•
• N•••••Ji.•••••
••
•
1 i	i
dau point. All phase transitions found are of second order
•	•	• •
1
NT-
• •
•
NT
•
NT+
except when more thNanT one order parameter acquires a non-
NT i=1
i=1
(11)
•
which approximate0s Eq. (10) by0.t4he correspon0d.8ing nonequi-1.2
0
0.4
0.8
1.2
occur at I − N , T − N , or I − N . A fuller account of the prop-
T
T
U
berties of this model is deferred to our future pΛublication.
librium MF afree energy
Λ
To check the validity of the MF predictions the phase
FIG. 2. (Color online) Phase diagram for τ = 28 . Lines represent
1 NdβFIGT.r3[.P(C(1ol)oVr o(n1l,in2e))PP(h2a)s]e diagNramTr[foPr (T1=)1l.nLPin(e1s)r]e.present
βF MF
diagrams were also determ2in8ed from MC 1s5imulations. The
= 2
+
neq
F
i
g
ur
e
4
.4
:
Ph
a
se
d
iag
r
a
m
s
fo
r
m
o
d
el
(
4
.
1
) for τ = 1 (a) and τ =
(b). In a) note the
MF res
ul
t
s;
po
in
ts
a
re
fro
m
M
C
s
i
m
u
lat
ion
s
fo
r
th
e
th
r
ee
mean-fiel
-
d results; points are from MC simulations for the three-
(1,2)
(1)
simulations were performed n a 16 X 16 X 16 lattice with
15o
−1
dimensional cubic lattice (16 X 16 X 16); t =(13E) .
(12)
1
dimenpsieornioadl iccu√bboicunldaattriyceco(1n6di×tio1n6s.×E1a6c)h.
MNoCtemtohvate ailnlclpuodsesdiblae
presence of the biaxial phase in the vicinity of λ =	. Observe that in b) the T phase
√
6
phasesrootfattihoenmoofdael mmoeleetcautleth’se oLraienndtaautiopnoinatn(dλa=p1a/rity6,intv=ers8i/o5n).,
exists in a very narrow temperature and that there exists a direct I − N ∗ transition for
Please noptaerathmaetteinrs MthFatthaecoqruyiroef noornieznertoatiaovnearlalgyeas nwd hterannsc-rossinwghich is surprisingly well reproduced in simulations. Continuous
T
The size of MC rotational moves was selected to produce an
1
lationally hovmaroioguesλnep=ohausse√ltirq.aunisditisotnrsu.ctIunreosrd, ewr htoerebewceonasvisetreangt ewith (Ldasheadc)cleipnteasnrceeprerasteinot fibresttw-oeredner 3(s0e%conadn-dord4e0r%) phinasethtreanosridtieornesd.
6
the interacti=o3n pernime(raagryyotbteottraaoihnbetedadriantbicyaonrLdeoefrnfepgcaatriavemetestaeinrl,.gwl[ee1-p]li.astrbtailcl–lerepmoaiinn-ts foprhaλse=s. T0y.p3i,c0al.l5y,, 510 00o0bttaoin2e0d0 0b0y0 MlatotinceteswCeaeprslowere
√
potential dueintgo (aslelcroenmdaariyn)inmgopleacrutilcalreso,rdthere pparerasmenecteersofoflartatincke L ..: 3.
used to thermalize the6 system and 60 000 to 200 000 sweeps
    simulat(i2o) n as prese(n2) ted in(3s) ection 4.5, rema
where p ∈ {1,p} and where
ining points and mean-field lines obtained
(2)
These are: (a) Li	for N ; (b) Li	and pLi	for N ; (c) pLi
s
for measurements. In the MC simulations, phase transitions
is reduced to a renormalization of the effective potential by
U
B
02
20
22
20
(2)
and pLi , along wi
th N secondary order paramet
ers, for N ;
c
in collaboratiU
on [119]. (a) reprinted witT
h permission from [1], Q
2009 by the American
were detected by observing the temperature dependence of
the number of nearest neighbors (d = 6
) for the si
mple cubic
22

r
*
1
and finally (d) for N all aforementioned order parameters
the order parameter
s. In (tLur)n, these q(uLa→ )ntities were deter-
)
Physical So
ciety. (b) c 2012 by the American Physical Society)
T
lattice considered here.
dQ pst., (Q) ps→ t.,	(Q)
(2)Q	(2)
→
are nonzero, in addition to ¯p, pLi00 , and pLi02 . Here
mined f2rom the asymptoticmbnehaviors ofmt→hn→e correlation func-
As usual, the equilibrium one-particle distribution function,
(Lp)±1
ˆ (L)
ˆ (L)
4.(
3 ) Mont�e Carlo simulations
tions Gmm'(li − jl)= Tm (Oi)· Tm'(Oj) and Gpp(li − jl)= pipj
MF
P , is obtained variationally b
2+o +o
y m
i
nimizing F	with respect
1
0m
0m
'
8π 2
eq
non
(L)
L
L
[o + (− 1) o	]D	,
for large li − jl. Here the overline indicates an ensemble av-
Li	=
to P (i), subject to the normalization condition Tr[P (i)]
= 1.
(17)
J
δLL→ δmm→ δnn→ δss→ .
ss
'
−ss
'	sms m
mm
'
' '
=
2
erage. In the simula(t2ioLns+, th1e) temperature resolution ot satis-
(i)
s,s'=±1
MF
The necessary condition for P , δF	/δP |
= λ, where
fied ot = 0.01. At the above resolution (and system’s size) our
(5)
eq
non
P =
P
eq
Pleasesiombusleatrivoensthwaet,reacucnoarbdleintgo tdoisEtinqg.u(i7s)h, bt.,et’ws edeenpewnedakolny Qfir.stI-f
λ is the Lagrange multiplier, becomes reduced to a Fredholm-
In the presented results a simple cubic lattice of N = 16 × 16 × 16 sites with nearest-
the coorrrdeesrpaonnddisnegcoonrdd-eorrdpearrpahmaseetetrrsanasrietions. The, wMhCerteransition
type nonlinewarheinreteDgraarleetqhueaWtioignn, er rotation matrices.
pst.,L
mn
We nareeingohwboinrpionstiteiornactotieovnalsuaatentdhepMerFioapdpircoxbimoautniodnaryccuorvneds iltieiobnesloiws tchoonsesiodbetariended. The temperature
from MF. The MF results
 worsen from a discrepancy of 8% to about 20% as A in-
to F and obtain the equilibriu
−1
m
ff properties of our system. We
−βdV (1)
P (1) = Z
(13)
MFe
e
,
1
r
eq
→ (N − N*). The I − N
crease from A = 0 (I −
s )
→N ) to A
→ = 0.3
have identified six stable phases of model (1) that cover the
scan progresses by heating, i.e. the initial lattice is prepared in aU
completely-oT
rdered N	U
∗
X
X(p,Q )P (p,Q )dQ	Tr[X P ],	(18)
T
T
pa=rt o2f our MC diagram agrees with M≡C results of Biscarini
whole symmetry reduction flowchart of Fig. 2. The phases
where
are (a) stthae tiesoitnroptihceplhoawsee; s(bt)ttehme upneiarxaitaul rperoalantedotrhoeblfiatneal steat tael. i[s2p1=p]±a. 1ssed down as an initial state for the
The liquid-crystal phases appear due to the combination
nematicsupbhsaeseq;u(ecn) tthseimbiuaxliaatl iophnasfeo; r(da) ltahergteertratheemdraptic
erature. At the beginning of the thermalization
V (1) = Tr[V (1,2)P (2)],
(14)
then the expansion for P (p,Q ) can be cast i
→
n the following
eff
eq
of octupol
ar interactions with qua
drupolar contributions. In
phase; (e) the prolate or oblate tetrahedratic nematic phase;
(2)
(f)prthoececshsiratlhteetrraahdeidurastiocf ntehmeartiacnpdhoamse. wEaxlekmpinlarrgyoetnaetraaiodl dnfiotsirompna:tcoearte(tarashdederfiatnicedneminat(i1c .p4h9a)sei,secxoismtinpguintepdrolate
and
ZMF = Tr[e−
(NT+) and oblate (NT−) versions, the NT phase appears stable.
9to matc(h1) an acceptance rate in the 40%
∼It 5d0oe%s nroat napgpee.ar fTorh2ALe=t0ho1errAm=aJl3iz, awthiiocnh ccoorrnesspiosntsd to a
uPni(apx,iQal→)lim=it. From the8πlea2dinpgsMt.,Fmmco→ nptsrit.,bumtmio→n(Qto).the (p1a9r-)
and where the equilibrium MF free enerIgy becomes
of 500000 lattice sweeps. Production
(equiliitbyroirudmer psatraaLmt,mee,tmesr→a,,sm¯p, panliningd)ucceod nhsoimstosgeonefou5s0c0h0ir0a0lity is
MF
1
Tr
[P •
(1)
(1)] − N ln Z
.	(1••6) •
βF	= − N
βd
V
seen to emerge when both biaxial and tetrahedratic orders
2lattice sweeps, while every tenth configuration is considered for calculating averages to
eq	eff
•
•	•	•
MF
•
•
•
•
eq
6
(1)
•
Assumcoinndgentshea.tTthheeesfitirmstatlioabnegliv(ems )
in p t.,L refers to the
•
correlations be•tween subsequent states. After the final state is pamsnsed onto
minimizTe
symmetry of the pJh2ase and the second (n) to the molecular
With the assumed
choice of mutual orient•ation of twofold
(3) (2)
(2) 3
axes of the molec3uthlee’s nQexatndsiTmtuelnastoirosnsifxorstaablNhe isgthruecrtutreems
perature, another21r0ot4und of 500000 thermalization
mn
T-
(or, equivalently, the order parameters pst.,L ) are nonvanish-
(Fig. 2 in LPW) are identified among stationary solutions
cycles follows, etc. The ensemble averages and susceptibilities are calculated in
ing fowr heiacchhvoafnitshheesprwevhieonusbliyaxiidael notrifiteetdrashterudrcattuticrheeos.rdsearmpearam-
mn
NT+
of Eq. (13): (a) the O(3)-symmet
ric, isotropic phase (I ); (b)
*
N
eters are zero. A maximal transition temperature to a chiral
T
the D∞h-symmetrimc uanninaxeiralapsroitlawtea(sNint)roandducoebdlatien(NCha)pter 3,(sap) eFcoifir etdheinI tphheasdeefithneitoionnlys n(3on.3v8an)isahnindg(3fu.3n9ct)i.on
is
phase is achieved for the self-dual point of A=1 J6.
00
U +
U − 1.2
0.4
0.8
= 1.
00
Λ
phase; (d) the T -symmetric tetrahedratic (T ) phase; (e) the
trial m(bo)evlFuesosirvoethntehNeNrmUroaptnrhodapsoicemsb,liayxicahl onseemnatmic oplheacseul[e1s5,,1w6]h, ialned re-
d
A lattice sweep consists of performing
D2d -symmetricF,IGdi.s4t.or(Cteodlotreotnralihnee)dMraFtipchnaseemdaiatgicramprofolraTte= 9(N(sTe+e )captions
veal a path to a series of spatially homogeneous but aniso-
(toNTFi−g.)a3p)h.MaSsiomensu;tlaeatinoCndsa(rhfel)orethtaerreiaDdli2fmfi-scyuolmvt emsinecctoernipcsa,riisctythsidreaoglfresesepofaratterloypicapliqpuliy(disn[1g7].\tOh2f+eδth0Mme+seeδ0tmlri→qoupidoslitsheamlgoostriintthermesti(nsgeeone is
and oblate
t.,(L)*
r
L
L L

D	+ (−1) D
*
nematic tetra
h
e
d
r
ati
cc
(d
Nens
)
e p
haasgela.ssy state. The N phase cannot be reached
the NT→ phase, which should emerge
→ from a nonchiral
→ liquid
fr
e
ed
o
m
on
∗
to
=	√
section 1.8.1) to the orientational and parity degrees of freedom. Namely,
as a result of s2pontaneous chiral symcmoentrsyidberreiankigng. The
mm
mm
m−
m
a
T
T
An imporbtyansttasntdeaprdinMseotrlovpionlgis Esiqm.u(l1at3io)niss. the identification of
ˆ
ˆ
l
L L
L
+ (−
1) D	+ D
(20)
trial orientational move {aˆ , b , cˆ } → {
aˆ , b , cˆ } for a particle i, th→ e
l	l	l
energy →
difference for
,
the order parameters. This is achieved by expanding the one-
i	i	i
−mm
−m−m
i	i	i
040701-3
particle distribution function P (Q) ≡ P (p,Q→) in the series of
symmetry-adapted, real, linear combinations of the Wigner’s
where m = 0, 0 � m→ � L, ps = 1, and where L and m→ are even. Terms with m→ = 0 and m→ /= 0 correspond to molecular uniaxial and molecular biaxial contributions, respectively. The
nonvanishing terms coming from the molecular tetrahedral part
L
L
rotation matrices D	[35] and real combinations of D ’s
m→ n→
mn
multiplied by the parity degree of freedom, p. We denote the
symmetry-adapted functions, orthogonal over O(3), as pst.,L ,
mn
011704-4
t
t
t

RAPID COMMUNICATIONS

Chapter 5. Tetrahedratic order and chiral symmetry breaking in a dispersion model of
liquid crystals
89
the potential (4.1) reads:
z=6
\

i(j)
1
2
(
\
ˆ
ˆ
ˆ
ˆ
∆Ei =
V ({
p
, (aˆ , b , cˆ )}, {p , (aˆ , b , cˆ )}
) − V ({p , (aˆ , b , cˆ )}
l	l	l
, {
p , (aˆ , b , cˆ )}) .
i	i	i	i
j	j	j	j
i
j	j	j	j
i	i	i
(4.9)
The energy difference upon a parity flip pi → −pi reads:
z=6
\

i(j)
1
2
(
\
V ({pi, (aˆi, ˆbi, cˆi)}, {pj, (aˆj , ˆbj , cˆj )}) − V ({−pi, (aˆi, ˆbi, cˆi)}, {pj, (aˆj , ˆbj , cˆj )}) .
(4.10)
∆Ei =
Note that there is no adjustable parameter which allows for an adjustment of the accep-
tance rate for parity moves. We could, in principle, limit the number of accepted moves by reducing the number of attempts, which is not necessary. However, we have no means of encouraging more parity moves to be accepted, which results in parity being frozen for long periods of time in low temperatures, as the relative energy difference associated with a single flip is becoming large. Because the starting configuration is homogeneously chiral, this problem does not affect the lowest temperatures, as the initial state is already close to equilibrium. In intermediate temperatures, however, the time scales for the dy- namics of parity are much larger than for rotational degrees of freedom, which causes the Monte Carlo sample for quantities linked to parity to experience non-negligible temporal correlations.
4.3.1
Susceptibilities
We investigate the previously defined uniaxial and biaxial order parameter susceptibil-
ities (or measures of order parameter fluctuations) (3.44) and (3.45), but also consider susceptibilities of tetrahedratic order and parity. They are defined analogously, in terms of instantaneous lattice averages, as in the definition (3.39):
2
2
χ = p˜ )
− p˜
) ,
(4.11)
p
M
M
I
˜(3)
˜(3)
˜(3)
˜(3)
2
χT(3)
= T2 · T2 )M −	T2 · T2 )M .
(4.12)
2
4.3.2
Correlation functions
Because of the suspicion that in lower temperatures there might exist domains of opposite
homogeneous chirality, the average parity (4.7) can also be obtained by considering a

Chapter 5. Tetrahedratic order and chiral symmetry breaking in a dispersion model of
liquid crystals
90
correlation function:
  i−j|→∞
Gpp(|i − j|) = pipj | −→	pi · pj = p2.
(4.13)
Because of the periodic boundary conditions, the limit for the argument of (4.13) is half
of the edge of the lattice L. By calculating p as:
p = IGpp(L/2),
(4.14)
we evade the error due to spatial correlations when calculating the lattice average parity.
4.3.3
Determining transition temperatures
The most pronounced phase transitions of (4.1) are the ones associated with tetrahedratic
ordering, i.e. the I − T (isotropic to tetrahedratic, not observed in simulations), I − NT
(isotropic to nematic tetrahedratic, see Figs. 4.8 and 4.10), I − N ∗ (isotropic to chiral
T
nematic tetrahedratic, see Fig. 4.9), NU −NT (nematic uniaxial to nematic tetrahedratic,
see Figs. 4.5 and 4.7) and NB − N ∗ (nematic biaxial to chiral nematic tetrahedratic,
T
see Fig. 4.6) transitions, which produce a very strong peak in the energy fluctuation
c (defined in (3.42)). Recall that the fluctuation of energy calculated for the biaxial model (3.1) was of the order 5 ∼ 7 at the I − NU phase transition for a similar system (see e.g. Fig. 3.6b). The same method of calculating c yields peaks of the order of 30 for the aforementioned transitions in (4.1) (see e.g. Fig. 4.6d). This often means that the peak at the I − NU and I − NB transitions is overshadowed by the peak at a tetrahedratic symmetry breaking transition, if they are close. Therefore, for these transitions we determine the temperature by peaks in χ0 and χ2 respectively, adjusting to agree with the behavior of order parameters.
The transitions involving spontaneous breaking of tetrahedratic symmetry produce pro-
nounced peaks in c and χT(3) , which provide excellent indication of the transition tem-
2
perature.
The most challenging are the transitions where spontaneous breaking of chiral symmetry
occurs separately from breaking of tetrahedratic symmetry, i.e. NT − N ∗ (T phase is
T
not observed in our results), observed for τ = 1, λ = 0.3 (Fig. 4.5), τ = 1, λ = 0.5 (Fig.
28 , λ
28 , λ
4.7), τ =
= 0.3 (Fig. 4.8) and τ =
= 0.5 (Fig. 4.10). Firstly, we fail to
15
15
detect any peak in c due to the transition. Secondly, the collection of equilibrium states
from which the averages and susceptibilities are calculated is significantly correlated with respect to parity due to large time-scales, resulting in lowered precision of determining p and χp. If a peak in χp is present and its position is unambiguous, we use it to

Chapter 5. Tetrahedratic order and chiral symmetry breaking in a dispersion model of
liquid crystals
91
determine the transition temperature. There are, however, cases where χp does not
exhibit an unequivocal peak and in these cases we resort to approximating the transition
temperature as the point, where p starts to increase in the N ∗ phase. Furthermore, q2
T
is linked to p through (4.8), which affects the behavior of the order parameters and χ2
in NT and N ∗ phases as well.
T
4.4
Results for τ = 1
This result is complementary to the phase diagram in Fig. 4.4a. The original result
is supplemented in this section by temperature scans presenting thermal behavior of
order parameters q0, q2, p and ∆(3), energy fluctuation c and susceptibilities χ0, χ2, χp
22
The results are presented in figures 4.5-4.7, where Monte Carlo transition
and
χT(3) .
2
temperatures are indicated. Below will follow a general description of the results, while
detailed comments on the behavior of the measured quantities are given in the captions
1
of figures: Fig. 4.5 for λ = 0.3, Fig. 4.6 for λ =	and Fig. 4.7 for λ = 0.5.
√6
1
The only instance of NB phase exists for λ =	(Fig. 4.6), where we have a direct
√6

(3)
second-order I − NB transition, evidenced by and increase in q0 and q2, while p and ∆22
parameters are zero. A peak in χ2 is also noted and used to determine the transition
≈ 1.2. A second-order phase transition to the	phase is subse-
temperature
tI−NB
N ∗
T
(3)
quently encountered as the temperature is lowered, evidenced by an increase in ∆22 and
peaks in χT(3)
and χp.
2
For the generic prolate (λ = 0.3, Fig. 4.5) and generic oblate (λ = 0.5 4.7) cases, as
the temperature is lowered, first a uniaxial nematic phase occurs, followed by a second- order transition to the nematic tetrahedratic NT phase. Because of the slow dynamics of parity and the fact that biaxial ordering in the presence of tetrahedratic order is linked to parity, p and q2 experience fluctuations due to long temporal correlations in the NT
phase, evidenced by the behavior of χp and χ2. The correlations continue to the
N ∗
T
phase, which is visible in χp, particularly in the case of λ = 0.3, however χp indicates
that these effects are less pronounced in low temperatures. The transition to the
N ∗
T
phase is second-order and is evidenced by an increase in p, q2 and a peak in χp, which
was used to determine the transition temperature.

Chapter 5. Tetrahedratic order and chiral symmetry breaking in a dispersion model of
liquid crystals
92
a
b
N ∗
∗
1
1
0.0014
∆(3)
q0
q2
22
0.8
0.0012
p
0.8
  χ
T(3)
0.6
0.001
2
0.6
0.4
0.0008
0.2
0.0006
0.4
0
0.0004
0.0002
0
0
0.6
0.8
1
t
1.2
1.4
0.6
0.8
1
t
1.2
1.4
c
d
NT
N ∗
NT +
NU +
I
∗
NT +
NU +
I
T
7e-05
0.00025
25
0.004
6e-05
0
5e-05
5
4e-05
3e-05
0
2e-05
1e-05
0
0
0
0.6
0.8
1
t
1.2
1.4
0.6
0.8
1
t
1.2
1.4
Figure 4.5: Monte Carlo results for τ
= 1 and λ
=
0.3. Obtained transition temper-
atures:
tI−NU +
≈ 1.18, tNU +−NT + ≈ 1.18, t
≈ 0.76 (marked as dashed vertical
N
−N
∗
T +
T
lines). Note that the
NU +
phase exists in a very narrow temperature range, hence the
peak in c (d) is not discernible from the NU + − NT + peak. Peaks of χ0 (c) at I − NU +
and NU + − NT + are merged together. We use the rightmost edge of the peak in χ0 to determine the transition temperature. Also note the fluctuating behavior of χ2 and χp
in the NT + phase and at the onset of N ∗ (c, d), explained in section 4.3.3.
T
a) Uniaxial and biaxial order parameters q0 and q2, as defined in (3.21).
∆(3)
b) Tetrahedral order parameter
calculated as (4.6), phase chirality calculated as
22
average parity p from (4.14) and susceptibility of tetrahedratic order parameter
calculated as (4.12).
χT(3)
2
Susceptibilities of uniaxial and biaxial order parameters χ0 and χ2, calculated as
(3.44) and (3.45).
Fluctuation of energy c calculated as (3.42) and susceptibility of parity order param- eter χp calculated as (4.11).
χ0
q0, q2
∆(3)
22 , p
χ2
c
χT(3)
χp
2

c χp

0.0035

0.003

0.0025

0.002

0.0015

0.001

0.0005

0

χ0 χ2

0.0002	2

0.00015	1

0.0001	1
5e-05	5

Chapter 5. Tetrahedratic order and chiral symmetry breaking in a dispersion model of
liquid crystals
93
a
b
N ∗
∗
1
1
0.0007
0.8
0.0006
0.6
0.0005

0.4
0.6
0.0004
q0
q2
0.2
0.0003
0
-0.2
0.2
0.0001
-0.4
0
0
-0.6
0.6
0.8
1
1.2
1.4
1.6
1.8
0.6
0.8
1
1.2
1.4
1.6
1.8
t
t
c
d
N ∗
NT
NB
I
NB
I
∗
T
7e-05
0.0009
0.0008
0.0007
0.0006
0.0005
0.0004
0.0003
0.0002
0.0001
0
30
0.0018
0.0016
0.0014
0.0012
0.001
0.0008
0.0006
0.0004
0.0002
0
6e-05
25
5e-05
20
4e-05
15
3e-05
10
2e-05
5
1e-05
0
0
0.6
0.8
1
1.2
1.4
1.6
1.8
0.6
0.8
1
1.2
1.4
1.6
1.8
t
t
1
Figure 4.6:
Monte Carlo results
for τ
=
1
and λ
=
. Obtained transition tempera-
√6
tures:
tI−NB
≈ 1.2, t
≈ 1.12. Note that the NB phase exists in a very narrow
N −N
∗
B
T
temperature range, therefore the peak in c for the I − NB transition is not discernible
from the one at NB − N ∗ transition.
T
a) Uniaxial and biaxial order parameters q0 and q2, as defined in (3.21).
∆(3)
b) Tetrahedral order parameter
calculated as (4.6), phase chirality calculated as
22
average parity p from (4.14) and susceptibility of tetrahedratic order parameter
calculated as (4.12).
χT(3)
2
Susceptibilities of uniaxial and biaxial order parameters χ0 and χ2, calculated as
(3.44) and (3.45).
Fluctuation of energy c calculated as (3.42) and susceptibility of parity order param- eter χp calculated as (4.11).
χ0
q0, q2
χ2
∆(3)
22 , p
c
χT(3)
χp
2

  c
  χp

  χ
0
χ2

  ∆(3)
22
p

2

Chapter 5. Tetrahedratic order and chiral symmetry breaking in a dispersion model of
liquid crystals
94
a
b
N ∗
NT
NT −
NU −
I
∗
NT −
NU −
I
T
1
0.002
0.4
q0
q2
0.2
0.8
0
0.6
-0.2
0.001
-0.4
0.4
-0.6
0.2
-0.8
-1
0
0
0.6
0.8
1
1.2
1.4
1.6
1.8
0.6
0.8
1
1.2
1.4
1.6
1.8
t
t
c
d
N ∗
NT −
NU −
I
NT
∗
NT −
NU −
I
T
8e-05
0.0006
18
16
14
0.012
7e-05
0.0005
0.01
6e-05
0.0004
0.008
12
10
5e-05
4e-05
0.0003
0.006
8
6
3e-05
0.0002
0.004
2e-05
4
2
0
0.0001
0.002
1e-05
0
0
0
0.6	0.8
1
1.2	1.4
1.6
1.8
0.6
0.8
1
1.2
1.4
1.6
1.8
t
t
Figure 4.7:
Monte Carlo results for τ = 1 and λ
= 0.5. Obtained transition tempera-
tures:
tI−NU −
≈ 1.4, tNU −−NT − ≈ 1.24, t
≈ 0.94. Note the fluctuating behavior
N
−N
∗
T −
T
of χ2 and χp in the NT + phase and at the onset of N ∗ (c, d), explained in section 4.3.3.
T
a) Uniaxial and biaxial order parameters q0 and q2, as defined in (3.21).
∆(3)
b) Tetrahedral order parameter
calculated as (4.6), phase chirality calculated as
22
average parity p from (4.14) and susceptibility of tetrahedratic order parameter
calculated as (4.12).
χT(3)
2
Susceptibilities of uniaxial and biaxial order parameters χ0 and χ2, calculated as
(3.44) and (3.45).
Fluctuation of energy c calculated as (3.42) and susceptibility of parity order param- eter χp calculated as (4.11).
χ0
q0, q2
χ2
∆(3)
22 , p
c
χp
χT(3)
2

c χp

χ0 χ2

∆(3)
22
p

T2

Chapter 5. Tetrahedratic order and chiral symmetry breaking in a dispersion model of
liquid crystals
95
28
15
4.5
Results for τ =
This result corresponds to the phase diagram in Fig. 4.4b. Temperature scans, including
behavior of order parameters q0, q2, p and ∆(3), energy fluctuation c and susceptibilities
22
χ0, χ2, χp and χT(3) are presented in figures 4.8-4.10, where transition temperatures are
2
indicated. The obtained transition temperatures have been indicated in Fig. 4.4b as
1
points for λ = 0.3, λ =	and λ = 0.5. Below will follow a general description of the
√6
results, while detailed comments on the behavior of the measured quantities are given
1
in the captions of figures: Fig. 4.8 for λ = 0.3, Fig. 4.9 for λ =	and Fig. 4.10 for
√6
λ = 0.5.
1
For λ =	the multicritical Landau point exists (Fig. 4.9), where there is a direct,
√6
sharply first-order transition from isotropic I to the chiral phase	at t
N ∗
≈ 1.57.
I−N
∗
T
T
All measured order parameters experience a discontinuous increase at this point.
For the generic prolate (λ = 0.3, Fig. 4.8) and generic oblate (λ = 0.5 4.10) cases, as the
temperature is lowered, a sharply first-order phase transition to the nematic tetrahedratic
∆(3)
NT phase occurs, evidenced by a discontinuous increase in
and q0, coupled with
22
peaks in c, χT(3)
and χ0. Because of the slow dynamics of parity in lower temperatures
2
and because of the fact that biaxial ordering in the presence of tetrahedratic order is
linked to parity, p and q2 experience fluctuations due to long temporal correlations in the NT phase, evidenced by the behavior of χp and χ2. The correlations continue to
the	phase, but wane in lower temperatures, which is visible in χp. The transition
N ∗
T
from NT to N ∗ is second-order and is evidenced by an increase in p and q2. In the case
T
of λ = 0.5 it was possible to unequivocally identify a peak in χp, however this was not possible for λ = 0.3 and an approximation is made by observing the temperature at which p begins to rise. Note that the T and NU − phases, predicted by mean-field theory
1
1
(see Fig. 4.4b) to precede the NT phase for λ <	and λ >	respectively, exist in a
√6
√6
very narrow temperature range and are not observed in simulation.

Chapter 5. Tetrahedratic order and chiral symmetry breaking in a dispersion model of
liquid crystals
96
a
b
N ∗
∗
1
1
0.0003
0.8
0.00025
0.8
0.6
0.0002
0.6
0.4
q0
0.00015
0.2
  q2
0.4
0.0001
0
0.2
-0.2
5e-05
-0.4
0
0
0.8
1
1.2
1.4
1.6
0.8
1
1.2
1.4
1.6
t
t
c
d
N ∗
∗
9e-05
0.00012
35
0.001
c
χp
8e-05
7e-05
6e-05
5e-05
4e-05
3e-05
2e-05
1e-05
0
30
0.0001
0.0008
25
8e-05
0.0006
  χ0
20
6e-05
  χ2
15
0.0004
4e-05
10
0.0002
2e-05
5
0
0
0
0.8
1
1.2
1.4
1.6
0.8
1
1.2
1.4
1.6
t
t
28
Monte Carlo results for τ =
and λ = 0.3.
Figure 4.8:
Obtained transition tempera-
15
tures:
tI−NT +
≈ 1.56, t
≈ 1.1. Note that the T phase, predicted by mean-field
N
−N
∗
T +
T
(Fig. 4.4b) remains undetected due to very narrow temperature range. Also note the
fluctuating behavior of χ2 and χp in the
NT +
phase and at the onset of
N ∗
(c, d),
T
explained in section 4.3.3. In this case t
(b).
was determined from the behavior of p
N	−N
∗
T +
T
a) Uniaxial and biaxial order parameters q0 and q2, as defined in (3.21).
∆(3)
b) Tetrahedral order parameter
calculated as (4.6), phase chirality calculated as
22
average parity p from (4.14) and susceptibility of tetrahedratic order parameter
calculated as (4.12).
χT(3)
2
Susceptibilities of uniaxial and biaxial order parameters χ0 and χ2, calculated as
(3.44) and (3.45).
Fluctuation of energy c calculated as (3.42) and susceptibility of parity order param- eter χp calculated as (4.11).
χ0
q0, q2
∆(3)
22 , p
χ2
c
χp
χT(3)
2

∆(3)
22
p
  χ
T(3)
2

Chapter 5. Tetrahedratic order and chiral symmetry breaking in a dispersion model of
liquid crystals
97
a
b
N ∗
∗
1
1
0.00016
0.8
0.00014
0.8
0.00012
0.6
0.0001
0.4

  ∆(3)
0.6
22
q0
q2
8e-05
0.2
p
0.4
  χ (3)
6e-05
0
T2
4e-05
-0.2
0.2
2e-05
-0.4
0
0
-0.6
0.8
1
1.2
1.4
1.6
0.8
1
1.2
1.4
1.6
t
t
c
d
N ∗
∗
3.5e-05
0.0006
18
0.0025
16
14
3e-05
0.0005
0.002
2.5e-05
0.0004
12
10
8
6
4
2
0
0.0015
  χ
0
2e-05
  c
0.0003
χ2
χp
1.5e-05
0.001
0.0002
1e-05
0.0005
0.0001
5e-06
0
0
0
0.8
1
1.2
1.4
1.6
0.8
1
1.2
1.4
1.6
t
t
28
1
Figure 4.9: Monte Carlo results for τ =	and λ =
. The multicritical point is found
√6
15
for t
≈ 1.57.
I−N
∗
T
a) Uniaxial and biaxial order parameters q0 and q2, as defined in (3.21).
∆(3)
b) Tetrahedral order parameter
calculated as (4.6), phase chirality calculated as
22
average parity p from (4.14) and susceptibility of tetrahedratic order parameter χT(3)
2
calculated as (4.12).
Susceptibilities of uniaxial and biaxial order parameters χ0 and χ2, calculated as
(3.44) and (3.45).
Fluctuation of energy c calculated as (3.42) and susceptibility of parity order param- eter χp calculated as (4.11).
χ0
q0, q2
χ2
∆(3)
22 , p
c
χp
χT(3)
2

Chapter 5. Tetrahedratic order and chiral symmetry breaking in a dispersion model of
liquid crystals
98
a
b
N ∗
∗
1
0.00014
0.4
0.2
0.8
0.0001
0
8e-05
-0.2
-0.4
6e-05
0.4
-0.6
4e-05
0.2
-0.8
2e-05
-1
0.8
1
1.2
1.4
1.6
1.8
0.8
1
1.2
1.4
1.6
1.8
t
t
c
d
N ∗
NT −
I
NT
NT −
I
∗
T
3.5e-05
0.0002
16
0.0025
0.002
0.0015
0.001
0.0005
0
0.8
1
1.2
1.4
1.6
1.8
0.8
1
1.2
1.4
1.6
1.8
t
t
28
Figure 4.10:
Monte Carlo results for τ =	and λ = 0.5.
Obtained transition temper-
15
atures:
tI−NT −
≈ 1.7, t
≈ 1.21. Note that the T phase, predicted by mean-field
N
−N
∗
T −
T
(Fig. 4.4b) remains undetected due to very narrow temperature range. Also note the
fluctuating behavior of χ2 and χp in the
explained in section 4.3.3.
NT −
phase and at the onset of
N ∗
(c, d),
T
a) Uniaxial and biaxial order parameters q0 and q2, as defined in (3.21).
∆(3)
b) Tetrahedral order parameter
calculated as (4.6), phase chirality calculated as
22
average parity p from (4.14) and susceptibility of tetrahedratic order parameter
calculated as (4.12).
χT(3)
2
Susceptibilities of uniaxial and biaxial order parameters χ0 and χ2, calculated as
(3.44) and (3.45).
Fluctuation of energy c calculated as (3.42) and susceptibility of parity order param- eter χp calculated as (4.11).
χ0
q0, q2
∆(3)
22 , p
χ2
c
χp
χT(3)
2

14

0.00015	12

10

0.0001	8
6
5e-05	4

2
0	0

c χp

3e-05

2.5e-05

2e-05

1.5e-05

1e-05

5e-06

0

  χ0
χ2

∆(3)
22
p

2

  q0
q2

Chapter 5. Tetrahedratic order and chiral symmetry breaking in a dispersion model of
liquid crystals
99
4.6
Discussion and summary
Two classes of phase diagrams for the model (4.1) have been studied by Monte Carlo
simulation, providing the dependence on temperature and model parameters λ and τ of order parameters, fluctuation of energy and susceptibilities (measures of fluctuation) of order parameters for typical prolate and oblate values (λ = 0.3 and λ = 0.5), as well as the highly-symmetric Landau point (self-dual point of the quadrupolar biaxial model
1
(3.1)), λ =	. The two studied values of τ pertain to the nematic-dominated phase
√6
diagram topology for τ � 1.54 (τ = 1) and the highly-symmetric value τ = 28 , for which
15
the multicritical Landau point is observed.
Apart from the phases existing in l = 2 model of biaxial nematics (3.1), two phases with
tetrahedratic ordering have been identified: nematic tetrahedratic NT and chiral nematic
T . The T phase was not accessible by simulation in the considered cases. For τ = 1
28
N ∗
it is not present on the phase diagram, while for τ =	its temperature range is too
15
narrow to allow identification of the phase.
In the NT phase spontaneous breaking of tetrahedratic symmetry was observed by mea-
suring the tetrahedratic order parameter ∆(3). The phase transition to NT also is seen to
22
produce pronounced peaks in the fluctuation of energy c and susceptibility of the tetrahe-
dratic order parameter χT(3) .
The N ∗ phase was identified by observing the spontaneous
T
2
breaking of chirality, measured in terms of average parity p. The chiral phase is observed
in all cases, however the transition temperature is highest for a highly biaxial molecular
1
quadrupolar moment (λ ≈	) and high tetrahedratic coupling (through τ ).
√6
The results need not apply exclusively to the speculated complexes of embrace-locked bent molecules, as in Fig. 4.1, and can be linked to cases where the leading terms in the dispersion interaction expansion are the quadrupolar and octupolar couplings. To provide a general correspondence, in the future also tetrahedratic coupling terms where the octupolar tensor’s twofold axes are rotated with respect to the twofold axes of the quadrupole need to be considered. However, the observed homogeneous chirality without the observation of twisted domains or macroscopic states seems unlikely in real compounds. (4.1) does not account for twisted structures because of the lack of spatially- dependent coupling (e.g. coupling of the quadrupolar or octupolar moments to lattice vectors). This type of coupling is accounted for when, in addition to E > 0, τ > 0 and λ > 0 in the general model (2.11) κ > 0, the case studied in Chapter 5.
The results also indicate that the investigation of spontaneous chirality breaking in liquid
crystals calls for new simulation methods. In our experience, brute-force increasing of the cycle count in a standard Metropolis algorithm provides less-than-satisfying output when compared to the increasing time and computer resource consumption when a discrete

Chapter 5. Tetrahedratic order and chiral symmetry breaking in a dispersion model of
liquid crystals
100
degree of freedom, such as parity, is taken into account. Therefore in the future methods
such as parallel tempering should be considered [123].

Chapter 5
Spatially modulated structures
To conclude this thesis with a promising, open problem, we explore a proposed extension
to the model (4.1) which, as we preview in this short chapter, produces spatially inhomo- geneous structures and ambidextrous chirality. Such an effect should be accounted for, considering the findings involving bent-core molecules [38–40, 43, 55] and flexible dimers [45–50].
5.1
Intermolecular vector coupling
The inclusion of uniaxial (D∞h), biaxial (D2h) and tetrahedral (Td) symmetries in the
model (4.1) permits one to construct an antisymmetric tensor using the symmetrized
irreducible tensors:
ˆbαn · (ˆbβn × ˆbγn) = 2√2
\

(x,y,z)∈π{α,β,γ}
T (2) T (2) T (3)
,
(5.1)
0,xµ 2,yν 2,µνz
where	= aˆn, ˆbyn = ˆbn, ˆbzn = cˆn are the molecular basis vectors for site n and the
ˆbxn
summation runs over cyclic permutations of {α, β, γ}, with Einstein summation conven-
tion assumed for the remaining indices. The lowest non-trivial term including this tensor
_rij
involves coupling with the intermolecular (or inter-site) versor rˆij =	(_rij = _rj − _ri),
rij
rˆij = −rˆji and one of the molecular moments present in the interaction (4.1). Consider-
ing the quadrupolar moment, one obtains [119]:
Vc(Ωˆ i, Ωˆ j ) = κE [ˆbαi · (ˆbβi × ˆbγi)Qαν (Ωˆ i)Qβν (Ωˆ j )
— ˆbαj · (ˆbβj × ˆbγj )Qαν (Ωˆ j )Qβν (Ωˆ i)l (rˆij )γ,
(5.2)
101

Chapter 6. Spatially modulated structures
102
where α, β, γ, ν = {x, y, z}, Qρδ (Ωˆ ) = (Q(Ωˆ )\
and Einstein summation convention is
ρδ
assumed. A similar term exists for the octupolar tensor:
ˆ
ˆ
ˆ
(3)
2 ανµ
(3)
V T
ˆ	ˆ
(Ω )T	βνµ(Ωˆ j )
ˆ
(Ω , Ω ) = κ E [ b
(b
× b
)T
i	j
T	αi	βi
γi
i
c
2
(5.3)
(Ωˆ j )T (3)	(Ωˆ i)l (rˆij )γ,
ˆ
ˆ
ˆ
(3)
2
— b
(b
× b
)T
αj	βj
γj
2
ανµ
βνµ
(Ωˆ ) = (T(3)(Ωˆ )\ . Terms (5.2) and (5.3) are invariant with respect to
T (3)
where
2
2
αρδ
ρδ
simultaneous inversion of both parities and an exchange of sites, i.e.:
V (T )
(pi, Ωˆ i, pj Ωˆ j ) = Vc	(−p , Ω , −p , Ω ).
(T )
ˆ
ˆ
(5.4)
l	l
l
l
j
i
c
j
i
5.2
Consequences of intermolecular vector coupling
We study a model defined by the pair interaction potential constructed by supplementing
the potential (4.1) with the quadrupolar variety of the lattice-coupling potential (5.2):
Vt(Ωˆ i, Ωˆ j ) = VT (Ωˆ i, Ωˆ j ) + Vc(Ωˆ i, Ωˆ j ).
(5.5)
We assume κ ≥ 0. The Hamiltonian is constructed on a lattice with nearest-neighbors
coupling:
N
1
H =	\ Vt(Ωˆ i, Ωˆ j ).
(5.6)
2
(i,j)
This model corresponds to the general model (2.11) for the case when the parameters
λ, E, τ and κ are non-zero. We do not specify which type of lattice is assumed, as three types are used: an open chain, a two-dimensional square lattice and a three-dimensional simple cubic lattice.
We will now consider the minimum of (5.5) for two isolated neighboring particles to
show that it favors a twisted state for non-zero κ. The simplest parametrization of (5.5)
is in relative Euler angles, i.e. Vt(Ωˆ i, Ωˆ j ) ≡ Vt(pi, pj, Ωˆ l ), where	= {αij, βij, γij }
Ωˆ l
ij
ij
defines the (proper) rotation, which carries	into Ωˆ l . Since i and j are fixed, for
Ωˆ l
j
i
Ωˆ l
Ωˆ
simplicity we assume	≡	= {α, β, γ}. For the sake of the argument we place the
ij
particle i at the origin and the intermolecular vector, which points at the particle j, is
parametrized in polar coordinates (θ, φ): rˆij = {sin(θ) cos(φ), sin(θ) sin(φ), cos(θ)}. In this parametrization, (5.5) reads:
Vt(pi, pj, Ωˆ l) = −E[fQQ(Ωˆ l) + τpipjfT T (Ωˆ l) + κ(pi + pj )fr (Ωˆ l, θ, φ)],
(5.7)

Chapter 6. Spatially modulated structures
103
where:
√
(2)
(2)
(2)
(2)
ˆ
ˆ
ˆ
ˆ
ˆ
2
f
(Ω ) = ∆	(Ω ) +	2λ[∆	(Ω ) + ∆	(Ω )] + 2λ ∆	(Ω ),
l
l
l
l
l
(5.8)
QQ
00
20
02
22
fT T (Ωˆ l) = ∆(3)(Ωˆ l),
(5.9)
22
1
fr (Ωˆ l, θ, φ) = {λ sin(2α cos(θ)[λ cos(2γ)(3 + cos(2β)) + √6 sin2(β)]+
2
+ λ sin(2γ)[sin(β) sin(θ)(2λ cos(α + φ) + √6 cos(α + φ))+
1
(5.10)
+ 4λ cos(2α) cos(β) cos(θ)] +	sin(2β) sin(θ)[sin(α − φ)×
2
√
√
× ( 6λ cos(2γ) − 3) − λ sin(α + φ)( 6 − 2λ cos(2γ))]},
∆(3)
(2)
(2)
ˆ
ˆ
ˆ
(Ω ), ∆	(Ω ) and ∆	(Ω ) are the symmetry-adapted Wigner functions (2.6), dis-
l
l
l
22
00
22
cussed in section 2.1.
For κ = 0 (and E > 0, τ > 0), the minimum of (5.7) is:
minVt(pi, pj, Ωˆ l) = −E(1 + 2λ2 + pipjτ ),
(5.11)
{Ωˆ I}
which is satisfied when pi = pj and the tetrahedral and quadrupolar twofold axes are
aligned in parallel. For κ /= 0, a competing minimum becomes global, which is achieved when the minor molecular axes aˆi and aˆj align in parallel along the vector rˆij , while the
ˆ
perpendicular molecular axes {bj, cˆj } are rotated along aˆj by an angle
β0ij ,
relative to
ˆ
{bi, cˆi}. The rotation is clockwise if pi = pj = 1 and counter-clockwise if pi = pj = −1.
The relative angle is given by:
κΛ(pi + pj ) Λ + 4τ
tan(2β0ij ) =
,
(5.12)
where:
Λ = 3 + 2λ(√6 + λ).
(5.13)
(5.12) can give a general idea on the macroscopic implications of the ground state, when
expanded in small κ. Upon ensemble-averaging the leading term, we obtain:
κΛ
β0ij ≈
p.
Λ + 4τ
(5.14)
It is now evident that the
N ∗
phase, i.e. when p /= 0, is unstable with respect to
T
spontaneous formation of twisted states and that the predictions of chapter 4 are valid
only in the κ = 0 limit. In the above approximation the twisted states have pitch of the
π
order of	. In other phases, where p = 0, from (5.12) we can conclude that local twisted
β0ij
domains of opposite handedness will form in equal abundance, leading to ambidextrous
chirality.

Chapter 6. Spatially modulated structures
104
Figure 5.1: Visualization of the octupolar and quadrupolar tensors on neighboring sites
in the twisted ground pair state configuration of (5.7) for λ = 0.4 and τ = κ = 1. (Image per [119], Qc 2012 by the American Physical Society.)
5.2.1
One-dimensional chain
The prediction (5.14) is very well supported by Monte Carlo simulations on a one-
dimensional open chain of molecules. We consider 32 sites aligned along the direction xˆ with free boundary conditions in all directions. The degrees of freedom are in no way limited with respect to the three-dimensional case, thus the molecules are free to rotate, as in previously considered cases.
We perform Monte Carlo simulations with the pair interaction potential (5.5) for τ =
1, λ = 0.3 and κ = 1. Considering homogeneous parity, p = 1, the estimation (5.14) gives β0ij ≈ 31◦ for mean relative clockwise twist about the molecular aˆ axes and a mean
π
pitch	≈ 5.8. As can be viewed in Fig. 5.2a, an equilibrium state after a 60000-cycle
β0ij
simulation for temperature t = 0.2, starting from an ordered state with homogeneous parity p = 1, confirms these predictions. The pitch is roughly equal to 6, while the mean
relative twist angle, averaged over the chain in the pictured configuration, is equal to
β0ij
≈ 30.8◦. On the other hand, simulation for a higher temperature shows domains of
opposite chirality with small but discernible twists, which confirms our predictions. (See
Fig. 5.2b.) However, it should be stressed that although overall parity p decreases as temperature is raised, there is no phase transition observed in the one-dimensional case, as it is known that for discrete symmetry groups no phase transitions exist for a chain with nearest-neighbors interaction in finite temperature.

Chapter 6. Spatially modulated structures
105
a
b
Figure 5.2: Result of a 60000-cycle Monte Carlo simulation of
(5.5) on an open-ended
one-dimensional chain of length 32 for t = 0.2 (a) and t = 0.5 (b) with τ = 1, λ = 0.3 and
κ = 1. The pictured rectangular cuboids represent the molecular quadrupolar moments
Q(Ωˆ ), while the color stands for parity: p = +1 (red) and p = −1 (green).
1. Global twisted state in the homochiral phase. The pitch of the global twist is esti- mated as ∼ 6, while the mean relative angle is β0ij ≈ 30.8◦ (averaged over the pictured configuration), which is in excellent agreement with the prediction (5.14).
2. Ambidextrous chiral domains in a disordered phase.
5.3
Two-dimensional lattice
Let us constrain the model (5.5) to a two-dimensional square lattice in the (xˆ, yˆ) plane
and let the boundary conditions in xˆ and yˆ directions be periodic, while keeping the boundary conditions free along zˆ. The molecular degrees of freedom remain as in the three-dimensional case, thus we are left with a free-standing single-layered film. For such a system the intermolecular vectors are constrained to four directions, i.e. rˆij =
{1, 0}, {0, 1}, {−1, 0}, {0, −1}.
Consider now that two molecules, 1 and 2, of identical parity p1 = p2 = +1, occupy neighboring sites at positions (x1, y1) = (0, 0) and (x2, y2) = (1, 0) (Fig. 5.3a). As discussed in the previous section, the ground state of such configuration is achieved when both molecules 1 and 2 align with aˆ1 aˆ2 rˆ12 = {1, 0} and molecule 2 is tilted clockwise with respect to 2 around aˆ2 (or vice-versa). Now consider a third molecule, 3, p3 = p1 = p2 = +1, located at (x3, y3) = (0, 1). If 1 and 3 were treated in isolation (Fig. 5.3b), the ground state would be achieved analogously, by aligning aˆ3 aˆ1 rˆ13 and tilting 3 clockwise with respect to 1 along aˆ3 (or vice-versa). Now notice that the two pairwise ground states for 1 and 2 and for 1 and 3 cannot be achieved simultaneously (Fig. 5.3c). Adding more molecules multiplies the number of conflicting conditions. Thus, the system is frustrated. The question of how the system relaxes this frustration is difficult to answer on analytical grounds and in the present we resort to simulation in search for an answer.
5.3.1
Simulations and results
We perform Monte Carlo simulations of the model (5.5) on a square 32 × 32 lattice with
periodic boundary conditions in the lattice plane and free boundary conditions in the perpendicular direction. We take λ = 0.3 and τ = κ = 1. Starting from an initial,

Chapter 6. Spatially modulated structures
106
a
b
c
Figure 5.3: Illustration of how frustration emerges in the model (5.5) when three instead
of two molecules with identical parity (p = +1) are considered. Molecules are represented by rectangular cuboids, which roughly correspond to the molecular quadrupolar tensors Q(Ωˆ ).
1. Ground state of two isolated molecules placed on neighboring lattice sites along xˆ.
2. Ground state of two isolated molecules placed on neighboring lattice sites along yˆ.
3. The two pairwise ground states a and b conflict each other.
completely ordered and righthanded (p = +1) configuration, we run a simulation of
60000 cycles for the lowest temperature (t0 = 0.2) and pass the final state as the initial state to the next temperature and iterate until t = 1.05 is reached with an increment of δt = 0.05. To compare the scale of the number of Monte Carlo cycles taken into account, consider that it amounts to average ∼ 60 lattice sweeps per particle on the 32×32 lattice, which is of similar order as ∼ 50 − 100 lattice sweeps per particle on the 16 × 16 × 16 lattices for 200000 − 500000 cycles considered in the previous chapter.
In two dimensions we do not expect any phase transition associated with the continuous (rotational) degrees of freedom. However, as discussed in chapter 4, the molecular parity, being a discrete, two-state degree of freedom, is an Ising-like variable. Therefore it is reasonable to expect a phase transition with spontaneous parity (chirality) breaking. Certainly, chiral ordering will consequently induce some level of biaxial and tetrahedral ordering, but this ordering is not due to spontaneous breaking of SO(3) symmetry. We monitor this phase transition by the fluctuation of energy c (3.42) and the susceptibility of the parity order parameter χp (4.11). Average parity is computed by direct ensemble averaging of the molecular parity p. All other quantities are computed as they have been in previous chapters.
The results indicate that, indeed, a phase transition between the disordered and chiral
states exists in two dimensions, at temperature tc ≈ 0.9 ∼ 0.95, characterized by a sharp drop in phase chirality p and peaks in c and χp as tc is approached from below (Fig. 5.4). This is an expected result, however what is more curious is the apparent existence of a phase transition within the chiral phase. It is visible as a minor peak in c (Fig. 5.4b) and a pronounced peak in the susceptibility of the uniaxial order parameter χ0 (3.44), as well as an increase in the uniaxial parameter q0 (3.21) as the temperature is raised

Chapter 6. Spatially modulated structures
107
a
b
5e-05
12
1
0.005
10
4e-05
0.8
0.004
8
3e-05
0.6
0.003
6
2e-05
0.4
0.002
4
1e-05
0.2
0.001
2
0
0
0
0.2
0.3
0.4	0.5	0.6	0.7	0.8	0.9
t
1
1.1
0.2
0.3	0.4	0.5	0.6	0.7	0.8	0.9
t
1
1.1
Figure 5.4: Several Monte Carlo quantities obtained from a simulation of model (5.5) on
a 32 × 32 lattice for λ = 0.3 and τ = κ = 1.

a) Phase chirality measured by average parity p, the primary uniaxial order parameter
q0 (3.21) and susceptibility of the uniaxial order parameter χ0 (3.44).
b) Fluctuation of energy c (3.42) and susceptibility of the chirality order parameter χp
(4.11).
(Fig. 5.4a), which indicates that some kind of reordering is taking place, approximately
at the temperature tr ≈ 0.55.
Investigation of the final lattice states reveals that for t < tr bent-wavefront-cholesteric structures exist, where the cholesteric-like wavefronts bend at right angles and do not form any defects, i.e. do not split or terminate (Fig. 5.5d). This structure apparently relaxes the frustration of the ground state, discussed in the previous section. We have found these states to be remarkably stable, as they form rapidly from the initial ordered state and throughout the simulation no qualitative changes are observed. For tc > t > tr two-dimensional cholesteric structures are found, where the molecules are aligned with their molecular aˆ axes in parallel to the diagonal of the lattice and rotate along aˆ (Fig. 5.5b). The pitch of such structure appears to agree with the prediction (5.14) in the xˆ
1	π
and yˆ directions, while along the diagonal it can be estimated as
, which for the
√2 (β0ij )
given parameters predicts a pitch of 4. Investigation of e.g. Fig. 5.5b shows that this
is indeed the case. Above tc, the disordered state is found with many small domains of opposite chirality (Fig. 5.5a). The ordered structures bear uncanny resemblance to the freeze-fracture imaging results obtained recently for the twist-bend nematic phase [50].
p, q0
χ0
c
χp

c χp

p q0 χ0

Chapter 6. Spatially modulated structures
108
a
b
c
d
Figure 5.5:
Final lattice states for the simulation of model (5.5) on a 32 × 32 lattice
for λ = 0.3 and τ = κ = 1, showing different structures for different temperatures. The
rectangular cuboids represent the molecular quadrupolar moments Q(Ωˆ ), while the color represents parity: p = +1 (red) and p = −1 (green).
1. t = 0.95: Ambidextrous chiral domains in the disordered state existing for t > tc.
2. t = 0.8: A two-dimensional cholesteric state with a wave vector parallel to the diagonal of the lattice. The molecules are aligned with their molecular aˆ axes in parallel, along which they rotate.
3. t = 0.55: Reordering transition in the chiral phase. At t = tr ≈ 0.55 cholesteric states found for tc > t > tr coexist with the bent-wavefront-cholesteric structures encountered for t < tr .
4. t = 0.25: Stable bent-wavefront-cholesteric structures existing for t < tr .
5.4
Three-dimensional lattice
The results for the two-dimensional version of model (5.5) raise the question whether
similar bent-wavefront structures, or perhaps even more complicated ones, will be ob- served in three dimensions. Clearly, the frustration of the ground state argued for the two-dimensional case should be more manifest in three dimensions. Our results in this respect are merely a teaser of what is possible in these systems, therefore we keep this section short and skip to presentation of the results.

Chapter 6. Spatially modulated structures
109
The simulations were carried out for a three-dimensional 16 × 16 × 16 simple cubic lattice
with periodic boundary conditions in all directions. We proceed in a similar manner as in the two-dimensional case, i.e. by first providing an initial, completely ordered state with p = +1 and passing the final state of each simulation for a given temperature as the initial state of the subsequent simulation for a higher temperature. The considered parameters are λ = 0.3 and κ = τ = 1, while the considered cycle count is 80000.
These preliminary results indicate that also in the case of a three-dimensional lattice,
complex, frustrated supramolecular states may exist. They have been found in the lower temperature regime, e.g. t = 0.2 and t = 0.4 (Fig. 5.6a and b), however for higher temperatures a periodic phase is also encountered, e.g. for t = 1.0 and t = 1.2 (Fig. 5.6c and d). As we see in Fig. 5.6c in particular, the molecules twist in a helix approximately along the diagonal and the pitch can be assessed by the modulating color to span only a few molecules. This kind of ordering is typical of the twist-bend nematic phase [42], while the surfaces of the simulation box in Fig. 5.6c and d can be, as in the 2D case, compared to the freeze-fracture imaging results obtained this year by the group at the University of Colorado in Boulder [50]. According to this account, the striped textures of the frozen samples do not indicate layering, but reflect the orientation of bent molecules forming helices. This is also visible in Fig. 5.6c and d.

Chapter 6. Spatially modulated structures
110
a
b
c
d
Figure 5.6:
Final lattice states for the simulation of model (5.5) on a simple cubic
16 × 16 × 16 lattice with periodic boundary conditions for λ = 0.3 and κ = τ = 1. The rectangular cuboids represent the molecular quadrupolar moments Q(Ωˆ ), while the color
represents parity: p = +1 (red) and p = −1 (green) with hue modulated by orientation of the molecular cˆ axes.
a,b) t = 0.2 and t = 0.4: Stable complex supramolecular structures.
c,d) t = 1.0 and t = 1.2: Stable layered phases.
5.5
Discussion
The preliminary results presented in this chapter indicate that the complex effects due
to spontaneous breaking of chirality, encountered e.g. in bent-core and flexible dimer systems can be accounted for in a microscopic dispersion model with a coupling to the intermolecular vectors, in the form such as (5.2). So far, such a model, in which twisted states and supramolecular structures form due to spontaneous breaking of chirality, has been missing. Subsequent detailed analysis needs to be undertaken to study the phase transitions and remaining unidentified structures, which can exist in other phases, in particular in the three-dimensional case. Finally, because geometrical frustration and chirality are known to lead to the emergence of blue phases, it is important to establish whether a link between the model (5.5) to those structures exists.

Chapter 6
Summary and conclusions
In the present thesis we have analyzed some of the cases described by the general model
(2.11) and have shown that it does reproduce many of the remarkable effects observed in bent-shaped liquid crystal molecules (bent-core, flexible dimer and ferrocene mesogens), such as field-stabilized biaxiality, homogeneous chirality, tetrahedratic order and twisted states of homogeneous and ambidextrous chirality. The results have been summarized in detail at the conclusions of the respective chapters, 3, 4, and 5. Herein we present a general comment on the results when viewed as a whole.
In general, the model studied in the present thesis, (2.11), produces many of the above
phenomena, such as field-stabilized biaxiality (as seen Chapter 3, in section 3.6.2, in particular Fig. 3.16), homogeneous chirality and tetrahedratic phases (Chapter 4, in sections 4.4 and 4.5), twisted helical states (in particular the three-dimensional result in section 5.4 in Chapter 5) and ambidextrous chirality (corroborated by 1D and 2D results in sections 5.2.1 and 5.3 in Chapter 5), as well as effects present in classic nematogens, such as the critical and tricritical points of the isotropic-uniaxial nematic transition (studied in detail in section 3.6.1 in Chapter 3). The stable biaxial nematic phase, which is present for no external field (see section 3.5) and also for τ > 0 (in particular see Fig. 4.6), has proved elusive in experiment and is widely believed to be unstable and is subject to constant experimental research at the time of completion of this thesis. Some cases of the model (2.11) however produce novel results, such as the field-induced decrease in
1
the isotropic-biaxial nematic transition temperature for the model (3.14) at λ =	(see
√6
the mean-field phase diagram in Fig. 3.18 and order parameter comparison in Figs. 3.19 and 3.20) and the apparent emergence of complex, frustrated supramolecular structures produced by the model (5.5), presented in Fig. 5.6 in Chapter 5, which bear resemblance
to the purported twist-bend nematic phase and blue phases.
111

Chapter 6. Summary and conclusions
112
Out of the vast number of possible cases we have investigated merely a few. Before
moving on to other ones than those considered in the present thesis, further investigation into the structures produced by the model (5.5), which we begin to explore in Chapter 5, is desirable. Other cases of great interest have been omitted here, which includes prominently the case of E > 0, λ > 0, τ > 0 and h > 0 in (2.11) (other parameters being equal to zero), in which the external field is expected to induce chirality in the nematic tetrahedratic (NT ) phase. Furthermore, if one additionally considers κ > 0, if field-induced chirality is indeed found, a possibility of field-triggered modulated structures opens, which clearly deserves attention for practical purposes.

Chapter 6. Summary and conclusions
113
Thanks
I would like to thank my supervisor, Prof. Lech Longa, for his teachings, support,
relentlessness, uplifting optimism and guidance throughout my studies.
I thank Dr. Tomasz Wydro for his indispensable help, company and many inspiring
discussions.

Bibliography
[1]
Longa, Pająk, and Wydro. Chiral symmetry breaking in bent-core liquid crystals.
Physical Review E, 79(4):040701, 2009.
[2]
de Gennes and Prost. The physics of liquid crystals. Clarendon Press (Oxford and
New York), 1993.
[3]
Neto and Salinas. The Physics of Lyotropic Liquid Crystals: Phase Transitions
and Structural Properties, volume 62. OUP Oxford, 2005.
[4]
Tolédano and Neto. Phase transitions in complex fluids. World Scientific Publishing
Company, 1998.
[5]
Reinitzer. Beiträge zur kenntniss des cholesterins. Monatshefte für Chemie/Chem-
ical Monthly, 9(1):421–441, 1888.
[6]
Lehmann. Über fliessende krystalle. Z. phys. Chem, 4:462–472, 1889.
[7]
Lehmann. Structure, system and magnetic behaviour of liquid crystals and their
miscibility in solid crystals. Annalen der Physik (series 4), 2:649–705, 1900.
[8]
Priestley and Wojtowicz. Introduction to liquid crystals. Plenum Publishing Cor-
poration, 1975.
[9]
Chandrasekhar. Liquid crystals. Cambridge University Press, 1992.
[10]
Vertogen and de Jeu.	Thermotropic liquid crystals, fundamentals, volume 45.
Springer-Verlag Berlin, 1988.
[11]
Heilmeier. Liquid-crystal display devices. Scientific American, 222:100–106, 1970.
[12]
Bahadur. Liquid crystal displays. Molecular Crystals and Liquid Crystals, 109(1):
3–93, 1984.
[13]
Chigrinov. Liquid crystal devices: physics and applications. Artech House Publish-
ers, 1999.
115

Bibliography
116
[14]
Boccara. Violation of rotational invariance and mesomorphic phase transitions
characterized by an order parameter. Annals of Physics, 76(1):72–79, 1973.
[15]
Tinh, Destrade, and Gasparoux. Nematic disc-like liquid crystals. Physics Letters
A, 72(3):251–254, 1979.
[16]
de Vries. Rotatory power and other optical properties of certain liquid crystals.
Acta Crystallographica, 4(3):219–226, 1951.
[17]
Meiboom, Sethna, Anderson, and Brinkman.
Theory of the blue phase of
cholesteric liquid crystals. Physical Review Letters, 46(18):1216–1219, 1981.
[18]
Kikuchi, Yokota, Hisakado, Yang, and Kajiyama. Polymer-stabilized liquid crystal
blue phases. Nature Materials, 1(1):64–68, 2002.
[19]
Yu and Saupe. Observation of a biaxial nematic phase in potassium laurate-1-
decanol-water mixtures. Physical Review Letters, 45(12):1000–1003, 1980.
[20]
Severing and Saalwächter.
Biaxial nematic phase in a thermotropic liquid-
crystalline side-chain polymer. Physical review letters, 92(12):125501, 2004.
[21]
Freiser. Ordered states of a nematic liquid. Physical Review Letters, 24(19):1041–
1043, 1970.
[22]
Hessel, Herr, and Finkelmann. Synthesis and characterization of biaxial nematic
side chain polymers with laterally attached mesogenic groups. Die Makromolekulare Chemie, 188(7):1597–1611, 1987.
[23]
Chandrasekhar, Sadashiva, Ratna, and Raja. A biaxial nematic liquid crystal.
Pramana-Journal of Physics, 30(5):L491–L494, 1988.
[24]
Praefcke, Kohne, Singer, Demus, Pelzl, and Diele. Thermotropic biaxial nematic
phases with negative optical character [1]. Liquid Crystals, 7(4):589–594, 1990.
[25]
Fan, Fletcher, Gündogan, Heaton, Kothe, Luckhurst, and Praefcke. The symmetry
of the nematic phase of a thermotropic liquid crystal: biaxial or uniaxial? Chemical physics letters, 204(5):517–523, 1993.
[26]
Li, Percec, Rosenblatt, and Lavrentovich. Biaxiality in a cyclic thermotropic ne-
matic liquid crystal. EPL (Europhysics Letters), 25(3):199, 1994.
[27]
Madsen, Dingemans, Nakata, and Samulski. Thermotropic biaxial nematic liquid
crystals. Physical review letters, 92(14):145505, 2004.
[28]
Merkel, Kocot, Vij, Korlacki, Mehl, and Meyer. Thermotropic biaxial nematic
phase in liquid crystalline organo-siloxane tetrapodes. Physical review letters, 93 (23):237801, 2004.

Bibliography
117
[29]
Acharya, Primak, and Kumar. Biaxial nematic phase in bent-core thermotropic
mesogens. Physical review letters, 92(14):145506, 2004.
[30]
Prasad, Kang, Suresh, Joshi, Wang, and Kumar. Thermotropic uniaxial and bi-
axial nematic and smectic phases in bent-core mesogens. Journal of the American Chemical Society, 127(49):17224–17227, 2005.
[31]
Lee, Lim, Kim, and Jin. Dynamics of electro-optical switching processes in surface
stabilized biaxial nematic phase found in bent-core liquid crystal. Journal of applied physics, 101(3):034105–034105, 2007.
[32]
Teixeira, Masters, and Mulder. Biaxial nematic order in the hard-boomerang fluid.
Molecular Crystals and Liquid Crystals, 323(1):167–189, 1998.
[33]
Galerne. Comment on “thermotropic biaxial nematic liquid crystals”. Physical
review letters, 96(21):219803, 2006.
[34]
Vanakaras and Photinos. Thermotropic biaxial nematic liquid crystals: Sponta-
neous or field stabilized? The Journal of chemical physics, 128:154512, 2008.
[35]
Matsuzaki and Matsunaga.
New mesogenic compounds with unconven-
tional molecular structures 1, 2-phenylene and 2, 3-naphthylene bis [4-(4-
alkoxyphenyliminomethyl) benzoates] and related compounds. Liquid Crystals, 14(1):105–120, 1993.
[36]
Takezoe and Takanishi. Bent-core liquid crystals: their mysterious and attractive
world. Japanese journal of applied physics, 45:597, 2006.
[37]
Francescangeli, Vita, Ferrero, Dingemans, and Samulski. Cybotaxis dominates the
nematic phase of bent-core mesogens: a small-angle diffuse x-ray diffraction study.
Soft Matter, 7(3):895–901, 2011.
[38]
Link, Natale, Shao, Maclennan, Clark, Körblova, and Walba. Spontaneous forma-
tion of macroscopic chiral domains in a fluid smectic phase of achiral molecules.
Science, 278(5345):1924–1927, 1997.
[39]
Xu, Selinger, Selinger, and Shashidhar. Monte carlo simulation of liquid-crystal
alignment and chiral symmetry-breaking. The Journal of Chemical Physics, 115: 4333, 2001.
[40]
Yan, Hixson, and Earl. Self-assembled chiral superstructures composed of rigid
achiral molecules and molecular scale chiral induction by dopants. Physical review letters, 101(15):157801, 2008.

Bibliography
118
[41]
Reddy and Tschierske. Bent-core liquid crystals: polar order, superstructural chi-
rality and spontaneous desymmetrisation in soft matter systems. Journal of ma- terials chemistry, 16(10):907–961, 2006.
[42]
Dozov.	On the spontaneous symmetry breaking in the mesophases of achiral
banana-shaped molecules. EPL (Europhysics Letters), 56(2):247, 2001.
[43]
Peroukidis, Vanakaras, and Photinos. Molecular simulation of hierarchical struc-
tures in bent-core nematic liquid crystals. Physical Review E, 84(1):010702, 2011.
[44]
Kim, Kadkin, Kim, and Choi. Tetrahedratic mesophases, ambidextrous chiral do-
mains and helical superstructures produced by achiral 1, 1’-disubstituted ferrocene derivatives. European Journal of Inorganic Chemistry, 2011(19):2933–2941, 2011.
[45]
Görtz, Southern, Roberts, Gleeson, and Goodby. Unusual properties of a bent-core
liquid-crystalline fluid. Soft Matter, 5(2):463–471, 2009.
[46]
Panov, Nagaraj, Vij, Panarin, Kohlmeier, Tamba, Lewis, and Mehl. Spontaneous
periodic deformations in nonchiral planar-aligned bimesogens with a nematic- nematic transition and a negative elastic constant. Physical review letters, 105 (16):167801, 2010.
[47]
Cestari, Diez-Berart, Dunmur, Ferrarini, de La Fuente, Jackson, Lopez, Luckhurst,
Perez-Jubindo, Richardson, et al. Phase behavior and properties of the liquid- crystal dimer 1”, 7”-bis (4-cyanobiphenyl-4’-yl) heptane: A twist-bend nematic liquid crystal. Physical Review E, 84(3):031704, 2011.
[48]
Henderson and Imrie. Methylene-linked liquid crystal dimers and the twist-bend
nematic phase. Liquid Crystals, 38(11-12):1407–1414, 2011.
[49]
Beguin, Emsley, Lelli, Lesage, Luckhurst, Timimi, and Zimmermann. The chirality
of a twist–bend nematic phase identified by nmr spectroscopy. The Journal of Physical Chemistry B, 116(27):7940–7951, 2012.
[50]
Chen, Porada, Hooper, Klittnick, Shen, Tuchband, Korblova, Bedrov, Walba,
Glaser, et al. Chiral heliconical ground state of nanoscale pitch in a nematic liquid crystal of achiral molecular dimers. Proceedings of the National Academy of Sciences, 110(40):15931–15936, 2013.
[51]
Lubensky and Radzihovsky. Theory of bent-core liquid-crystal phases and phase
transitions. Physical Review E, 66(3):031704, 2002.
[52]
Mettout. Macroscopic and molecular symmetries of unconventional nematic phases.
Physical Review E, 74(4):041701, 2006.

Bibliography
119
[53]
Wiant, Neupane, Sharma, Gleeson, Sprunt, Jakli, Pradhan, and Iannacchione.
Observation of a possible tetrahedratic phase in a bent-core liquid crystal. Physical Review E, 77(6):061701, 2008.
[54]
Weissflog, Schröder, Diele, and Pelzl. Field-induced formation of the polar smcp
phase above the smcp–isotropic transition. Advanced Materials, 15(7-8):630–633, 2003.
[55]
Brand, Pleiner, and Cladis. Tetrahedratic cross-couplings: novel physics for banana
liquid crystals. Physica A: Statistical Mechanics and its Applications, 351(2):189– 197, 2005.
[56]
Eisenshitz and London. Zeitschrift für Physik, 60:491, 1930.
[57]
Buckingham, Fowler, and Hutson. Theoretical studies of van der waals molecules
and intermolecular forces. Chemical Reviews, 88(6):963–988, 1988.
[58]
Buckingham. Theory of long-range dispersion forces. Discuss. Faraday Soc., 40:
232–238, 1965.
[59]
Maier and Saupe. Eine einfache molekulare Theorie des nematischen kristallinflüs-
sigen Zustandes. Zeitschrift Naturforschung Teil A, 13:564, July 1958.
[60]
Maier and Saupe. Eine einfache molekularstatistische Theorie der nematischen
kristallinflüssigen Phase. Teil I. Zeitschrift Naturforschung Teil A, 14:882, October 1959.
[61]
Maier and Saupe.	Eineeinfache molekularstatistische Theorie der nematischen
kristallinflüsign Phase. Teil II. Zeitschrift Naturforschung Teil A, 15:287, April 1960.
[62]
Onsager. The effects of shape on the interaction of colloidal particles. Annals of
the New York Academy of Sciences, 51(4):627–659, 1949.
[63]
Luckhurst, Zannoni, Nordio, and Segre.	A molecular field theory for uniaxial
nematic liquid crystals formed by non-cylindrically symmetric molecules. Molecular Physics, 30(5):1345–1358, 1975.
[64]
Luckhurst and Romano. Computer simulation studies of anisotropic systems: Ii.
uniaxial and biaxial nematics formed by non-cylindrically symmetric molecules.
Molecular Physics, 40(1):129–139, 1980.
[65]
Lebwohl and Lasher.	Nematic-liquid-crystal order—a monte carlo calculation.
Physical Review A, 6(1):426, 1972.

Bibliography
120
[66]
Fabbri and Zannoni. A monte carlo investigation of the lebwohl-lasher lattice
model in the vicinity of its orientational phase transition. Molecular Physics, 58 (4):763–788, 1986.
[67]
Straley. Ordered phases of a liquid of biaxial particles. Physical Review A, 10:
1881–1887, 1974.
[68]
Oseen. Arkiv matematik astron. Fysik A19, 1, 1925.
[69]
Frank. I. liquid crystals. on the theory of liquid crystals. Discuss. Faraday Soc.,
25:19–28, 1958. doi: 10.1039/DF9582500019. URL http://dx.doi.org/10.1039/ DF9582500019.
[70]
Gramsbergen, Longa, and de Jeu. Landau theory of the nematic-isotropic phase
transition. Physics Reports, 135(4):195–257, 1986.
[71]
Longa and Pająk. Luckhurst–romano model of thermotropic biaxial nematic phase.
Liquid crystals, 32(11-12):1409–1417, 2005.
[72]
Allender and Longa. Landau–de gennes theory of biaxial nematics reexamined.
Physical Review E, 78(1):011704, 2008.
[73]
Greiner, Neise, Stöcker, and Rischke. Thermodynamics and statistical mechanics,
volume 1. Springer-Verlag New York, 1995.
[74]
Huang. Introduction to statistical physics. CRC Press, 2001.
[75]
Metropolis and Ulam. The monte carlo method. Journal of the American statistical
association, 44(247):335–341, 1949.
[76]
Metropolis, Rosenbluth, Rosenbluth, Teller, and Teller. Equation of state calcu-
lations by fast computing machines. The journal of chemical physics, 21:1087, 1953.
[77]
Heard. Rigid body mechanics. Wiley-VCH, 2008.
[78]
Marsaglia. Choosing a point from the surface of a sphere. The Annals of Mathe-
matical Statistics, 43(2):645–646, 1972.
[79]
Podlozhnyuk. Parallel mersenne twister. NVIDIA white paper, 2007.
[80]
Durst. Using linear congruential generators for parallel random number generation.
In Proceedings of the 21st conference on Winter simulation, pages 462–466. ACM, 1989.

Bibliography
121
[81]
Hortensius, McLeod, and Card. Parallel random number generation for vlsi systems
using cellular automata. Computers, IEEE Transactions on, 38(10):1466–1473, 1989.
[82]
Marsaglia. Yet another rng, 1994. URL https://groups.google.com/forum/
?fromgroups=#!topic/sci.stat.math/p7aLW3TsJys.
[83]
Goresky and Klapper. Efficient multiply-with-carry random number generators
with maximal period. ACM Transactions on Modeling and Computer Simulation (TOMACS), 13(4):310–321, 2003.
[84]
Gratton. Parallel random number generation. URL http://www.ast.cam.ac.uk/
~stg20/cuda/random/.
[85]
Brink and Satchler. Angular momentum. Clarendon Press Oxford, 1993.
[86]
Jerphagnon, Chemla, and Bonneville. The description of the physical properties of
condensed matter using irreducible tensors. Advances in Physics, 27(4):609–650, 1978.
[87]
Mulder. Isotropic-symmetry-breaking bifurcations in a class of liquid-crystal mod-
els. Physical Review A, 39(1):360, 1989.
[88]
Acharya, Primak, Dingemans, Samulski, and Kumar. The elusive thermotropic
biaxial nematic phase in rigid bent-core molecules. Pramana, 61(2):231–237, 2003.
[89]
Olivares, Stojadinovic, Dingemans, Sprunt, and Jákli. Optical studies of the ne-
matic phase of an oxazole-derived bent-core liquid crystal. Physical Review E, 68 (4):041704, 2003.
[90]
Shimbo, Gorecka, Pociecha, Araoka, Goto, Takanishi, Ishikawa, Mieczkowski, Go-
mola, and Takezoe. Electric-field-induced polar biaxial order in a nontilted smectic phase of an asymmetric bent-core liquid crystal. Physical review letters, 97(11): 113901, 2006.
[91]
Francescangeli, Stanic, Torgova, Strigazzi, Scaramuzza, Ferrero, Dolbnya, Weiss,
Berardi, Muccioli, et al. Ferroelectric response and induced biaxiality in the ne- matic phase of bent-core mesogens. Advanced Functional Materials, 19(16):2592– 2600, 2009.
[92]
Nagaraj, Panarin, Manna, Vij, Keith, and Tschierske. Electric field induced bi-
axiality and the electro-optic effect in a bent-core nematic liquid crystal. Applied Physics Letters, 96(1):011106–011106, 2010.

Bibliography
122
[93]
Dunmur, Szumilin, and Waterworth. Field-induced biaxiality in nematics. Molec-
ular Crystals and Liquid Crystals, 149(1):385–392, 1987.
[94]
Barberi, Ciuchi, Durand, Iovane, Sikharulidze, Sonnet, and Virga. Electric field
induced order reconstruction in a nematic cell. The European Physical Journal E, 13(1):61–71, 2004.
[95]
Borshch, Shiyanovskii, and Lavrentovich. Electric field induced biaxial order and
differential quenching of uniaxial fluctuations in a nematic with negative dielectric anisotropy. Molecular Crystals and Liquid Crystals, 559(1):97–105, 2012.
[96]
Palffy-Muhoray and Dunmur.	Field-induced order in nematic liquid crystals.
Molecular Crystals and Liquid Crystals, 97(1):337–349, 1983.
[97]
Remler and Haymet. Phase transitions in nematic liquid crystals: a mean-field
theory of the isotropic, uniaxial, and biaxial phases.	The Journal of Physical Chemistry, 90(21):5426–5430, 1986.
[98]
Carlsson and Leslie. Behaviour of biaxial nematics in the presence of electric and
magnetic fields: Evidence of bistability. Liquid Crystals, 10(3):325–340, 1991.
[99]
Berardi, Orlandi, and Zannoni. Columnar phases and field induced biaxiality of
a gay–berne discotic liquid crystal. Physical Chemistry Chemical Physics, 2(13): 2933–2942, 2000.
[100]
Berardi, Muccioli, and Zannoni. Field response and switching times in biaxial
nematics. The Journal of chemical physics, 128(2):024905–024905, 2008.
[101]
Peroukidis, Karahaliou, Vanakaras, and Photinos. Biaxial nematics: symmetries,
order domains and field-induced phase transitions†. Liquid Crystals, 36(6-7):727– 737, 2009.
[102]
Jose, Jayasri, Dhara, Murthy, and Sastry. Effect of external field on the nematic
to isotropic transition: An entropic sampling study. Molecular Crystals and Liquid Crystals, 545(1):168–1392, 2011.
[103]
Trojanowski, Allender, Longa, and Kuśmierz. Theory of phase transitions of a
biaxial nematogen in an external field. Molecular Crystals and Liquid Crystals, 540(1):59–68, 2011.
[104]
Biscarini, Chiccoli, Pasini, Semeria, and Zannoni. Phase diagram and orientational
order in a biaxial lattice model: A monte carlo study. Physical review letters, 75 (9):1803–1806, 1995.

Bibliography
123
[105]
Chiccoli, Pasini, Semeria, and Zannoni. A detailed monte carlo investigation of
the tricritical region of a biaxial liquid crystal system. International Journal of Modern Physics C, 10(02n03):469–476, 1999.
[106]
Sonnet, Virga, and Durand. Dielectric shape dispersion and biaxial transitions in
nematic liquid crystals. Physical Review E, 67(6):61701, 2003.
[107]
Bisi, Virga, Gartland Jr, De Matteis, Sonnet, and Durand. Universal mean-field
phase diagram for biaxial nematics obtained from a minimax principle. Physical Review E, 73(5):051709, 2006.
[108]
Longa, Grzybowski, Romano, and Virga. Minimal coupling model of the biaxial
nematic phase. Physical Review E, 71(5):051714, 2005.
[109]
Allender, Lee, and Hafiz. Landau theory of biaxial and uniaxial nematic liquid
crystals. Molecular Crystals and Liquid Crystals, 124(1):45–52, 1985.
[110]
Meyer. Piezoelectric effects in liquid crystals. Physical Review Letters, 22(18):
918–921, 1969.
[111]
Hahn. Cuba—a library for multidimensional numerical integration. Computer
Physics Communications, 168(2):78–95, 2005.
[112]
Swendsen. How the maximum step size in monte carlo simulations should be
adjusted. Physics Procedia, 15:81–86, 2011.
[113]
Helfrich. Effect of electric fields on the temperature of phase transitions of liquid
crystals. Physical Review Letters, 24(5):201–203, 1970.
[114]
Rosenblatt. Magnetic field dependence of the nematic-isotropic transition temper-
ature. Physical Review A, 24:2236–2238, 1981.
[115]
Rosenblatt. Search for a field-induced nematic-isotropic critical point. Physical
Review A, 25:1239–1242, 1982.
[116]
Nicastro and Keyes.	Electric-field-induced critical phenomena at the nematic-
isotropic transition and the nematic-isotropic critical point. Physical Review A, 30(6):3156, 1984.
[117]
Walba, Körblova, Shao, Maclennan, Link, Glaser, and Clark. A ferroelectric liquid
crystal conglomerate composed of racemic molecules. Science, 288(5474):2181– 2184, 2000.
[118]
Longa and Pająk. Generalized dispersion model of orientationally ordered phases of
bent–core liquid crystals. Molecular Crystals and Liquid Crystals, 541(1):152–390, 2011.

Bibliography
124
[119]
Trojanowski, Pająk, Longa, and Wydro. Tetrahedratic mesophases, chiral order,
and helical domains induced by quadrupolar and octupolar interactions. Physical Review E, 86(1):011704, 2012.
[120]
Brand and Pleiner. Macroscopic behavior of non-polar tetrahedratic nematic liquid
crystals. The European Physical Journal E, 31(1):37–50, 2010.
[121]
Fel. Tetrahedral symmetry in nematic liquid crystals. Physical Review E, 52(1):
702, 1995.
[122]
Romano. Computer simulation study of a simple tetrahedratic mesogenic lattice
model. Physical Review E, 77(2):021704, 2008.
[123]
Swendsen and Wang. Replica monte carlo simulation of spin-glasses. Physical
Review Letters, 57(21):2607–2609, 1986.