Carbohydrate Polymers 290 (2022) 119486
Contents lists available at ScienceDirect
Carbohydrate Polymers
ELSEVIER
# Newly crosslinked chitosan- and chitosan-pectin-based hydrogels with high antioxidant and potential anticancer activity
Michal Dziadek a,b,*5 Kinga Dziadek c, Szymon Salagierskib, Mariola Drozdowska c,
Andrada Serafim d, Izabela-Cristina Stancud, Piotr Szatkowskie, Aneta Kopec c, Izabella Rajzerf,
Timothy E.L. Douglas g,h, Katarzyna Cholewa-Kowalskab
a Faculty of Chemistry, Jagiellonian University, Krakow, Poland
b Department of Glass Technology and Amorphous Coatings, AGH University of Science and Technology, Krakow, Poland
c Department of Human Nutrition and Dietetics, University of Agriculture in Krakow, Krakow, Poland
d Advanced Polymer Materials Group, University Politehnica of Bucharest, Bucharest, Romania
e Department of Biomaterials and Composites, AGH University of Science and Technology, Krakow, Poland
f Department of Mechanical Engineering Fundamentals, ATH University of Bielsko-Biala, Bielsko-Biała, Poland
g Engineering Department, Lancaster University, Lancaster, United Kingdom
h Materials Science Institute (MSI), Lancaster University, Lancaster, United Kingdom
ARTICLE INFO
ABSTRACT
Monoaldehydes, due to natural origin and therapeutic activity, have attracted great attention for their ability to
crosslink chitosan hydrogels for biomedical applications. However, most studies have focused on single-
component hydrogels. In this work, chitosan-based hydrogels, crosslinked for the first time with 2,3,4-trihydrox-
ybenzaldehyde (THBA), were modified with pectin (PC), bioactive glass (BG), and rosmarinic acid (RA). All of
these were not only involved in the crosslinking, but also modulated properties or imparted completely new ones.
THBA functioned as a crosslinker, resulting in improved mechanical properties, high swelling capacity and
delayed degradation and also imparted high antioxidant activity and antiproliferative effect on cancer cells
without cytotoxicity for normal cells. Hydrogels containing PC showed enhanced mechanical strength, while the
combination with BG gave improved stability in PBS. All hydrogels modified with BG exhibited the ability to
mineralise in SBF. The addition of RA enhanced antioxidant and anticancer activities and promoting the min-
eralisation process.
# 1. Introduction
Hydrogel materials are able to absorb large amounts of water and
swell without dissolving in aqueous media. These unique properties
hydrogels owe to three-dimensional crosslinked network of hydrophilic
polymer chains. Recently, hydrogels have attracted great attention for
their potential application in a wide range of biomedical areas, including
tissue engineering and controlled drug delivery systems. This is due to
the fact that hydrogels are able to mimic biomechanical characteristics
of native extracellular matrix (ECM), providing 3D microenvironments
for cell migration, adhesion, and proliferation, as well as promoting the
transport of nutrients and signalling molecules. Furthermore, their
porosity, high swelling ability, and hydrophilic nature make hydrogels
excellent candidates as carriers of hydrophilic biologically active
compounds (e.g. drugs, biomolecules, phytochemicals). Generally, all of
these properties of hydrogels are highly associated with the degree of
crosslinking (Mallick et al., 2020; Zhang et al., 2021).
Chitosan (CS), as a glucosamine-based polysaccharide obtained by
deacetylation of chitin, is one of the most studied biopolymers in the
biomedical applications. CS is characterised by good biocompatibility,
biodegradability, inherent antibacterial activity, hemostatic potential,
wide availability, and low price (Coimbra et al., 2011). Although CS-
based hydrogels for biomedical applications have been widely studied
in recent years, their effective and safe crosslinking still remains a great
challenge.
The most frequently used crosslinking agents of CS are dialdehydes,
in particular glutaraldehyde (GA). The crosslinking mechanism of dia-
ldehydes, including GA, is based on the formation of imine bonds, well-
* Corresponding author at: Faculty of Chemistry, Jagiellonian University, Krakow, Poland
E-mail addresses: michal.dziadek@uj.edu.pl, dziadek@agh.edu.pl (M. Dziadek).
https://doi.org/10.1016/j.carbpol.2022.119486
Received 16 September 2021; Received in revised form 30 March 2022; Accepted 12 April 2022
Available online 16 April 2022
0144-8617/© 2022 The Authors. Published by Elsevier Ltd. This is an open access article under the CC BY license (http://creativecommons.org/licenses/by/4.0/).
journal homepage: www.elsevier.com/locate/carbpol
Keywords:
Monoaldehyde
Polyelectrolyte complex
Bioactive glass
Polyphenols
micro-computed tomography

M. Dziadek et al.
Carbohydrate Polymers 290 (2022) 119486
known as Schiff bases, between two aldehyde groups of GA and amino
groups of chitosan chains. However, GA is highly cytotoxic and neuro-
toxic. In recent years, great interest has been focused on monoaldehydes
as CS crosslinking agent, which in many cases, unlike dialdehydes, are
naturally occurring compounds with beneficial biological activities (e.g.
antioxidant, anticancer, antibacterial) (Iftime et al., 2017; Xu et al.,
2018). The crosslinking mechanism of the monoaldehyde is based on
imine-bond formation between the single aldehyde group of the mon-
oaldehyde molecule and the amino group of the CS chain accompanied
by the hydrophilic/hydrophobic assembling of the CS/aromatic units of
the monoaldehyde. The monoaldehyde hydroxyl group in the ortho
position can form an intramolecular hydrogen bond with the imine ni-
trogen, providing the stabilization of the imine linkage (Iftime et al.,
. Furthermore, the hydroxyl groups in other positions can form
additional hydrogen bonds with the hydroxyl or the amino groups in
chitosan chains, enhancing the crosslinking effect (Xu et al., 2018).
The second important crosslinking mechanism of CS is ionic/elec-
trostatic interaction. Examples of this are polyelectrolyte complexes
(PECs), which are formed by electrostatic interactions between cationic
amino groups in CS and anionic groups in other polymers, such as
carboxyl acid groups of pectin (PC) under specific pH conditions (in the
pKa range of these two polymers) (Maciel et al., 2015).
PCs are anionic polysaccharides derived mainly from by-products of
the fruit processing industry, therefore they are environmentally
friendly, available in vast amounts and inexpensive (Neves et al., 2015).
PCs show good biocompatibility and biodegradability, as well as a wide
range of biological activities, such as anti-inflammatory, antioxidant,
and anticancer properties (Cui et al., 2017; Munarin et al., 2011; Neves
et al., 2015). PCs, especially low esterified amidated ones, can easily be
crosslinked by calcium ions to form hydrogels, also injectable systems
(Yuliarti et al., 2017). For these reasons, PCs are receiving increased
attention as a hydrogel material for drug delivery and tissue engineering
applications (Cui et al., 2017; Douglas et al., 2019; Munarin et al., 2011;
Neves et al., 2015).
A combination of CS and PC to obtain PEC hydrogels exploits the
biological benefits of both biopolymers while also enabling modification
of the material properties, such as mechanical behaviour, wettability,
swelling, and degradation (Chen et al., 2010; Coimbra et al., 2011). CS/
PC-based hydrogels showed high cytocompatibility with many cell types
(Birch et al., 2015; Li et al., 2010), capacity to be loaded with drugs
(Luppi et al., 2010; Neufeld & Bianco-Peled, 2017) and natural biolog-
ical active compounds (Maciel et al., 2015), indicating high potential in
biomedical applications.
In order to improve the biological and physicochemical properties of
hydrogels or impart completely new functionalities to them, various
additives are used. One of them is bioactive ceramic, especially bioactive
glass (BG). BGs have significantly altered the properties of hydrogels
relevant for bone regeneration applications (mechanical properties,
microstructural/topographical features, osteoblast activity) (Dziadek,
Charuza, et al., 2021a). Furthermore, calcium phosphate (CaP) forming
ability of BGs and osteogenic properties of their dissolution products (i.
e. silica, calcium ions) have induced hydrogel mineralisation with a CaP
phase, assuring improved mechanical properties, direct chemical
bonding with bone, and stimulation of bone regeneration (Sitarz et al.,
2013; Wajda et al., 2016, 2018). Other additives used in hydrogels are
biologically active compounds. In recent years, much attention has been
paid to naturally occurring chemicals - polyphenols, as alternative for
drugs and biomolecules. This is due to the multiple biological activities
of polyphenols, such as antioxidant, anticancer, anti-inflammatory,
antimicrobial and osteostimulation properties, and minor side effects
(Dziadek, Dziadek, et al., 2021b). One of the polyphenols frequently
found in herbal plants is rosmarinic acid (RA). RA has exhibited multi-
faceted activity, for instance strong antioxidant, anticancer, and anti-
inflammatory activities (Kuhlmann & Röhl, 2008; Xavier et al., 2009).
Furthermore, RA has been shown to regulate bone metabolism by
inducing osteoblast differentiation and inhibiting osteoclast activity
(Lee et al., 2015).
As we have shown in previous work, calcium-rich sol-gel-derived BG
particles can be a sufficient rich source of Ca2+ ions for internal cross-
linking of low esterified amidated PC (Douglas et al., 2019). Further-
more, numerous silanol groups (Si-OH) of sol-gel-derived BG and
hydroxyl groups of polyphenolic compounds may interact with each
other and also with functional moieties of chitosan (-OH, -NH2) and
pectin (-OH, -COOH) to form hydrogen bonds (Douglas et al., 2017;
Dziadek, Dziadek, et al., 2021b; Hu et al., 2021).
In this work, the phenolic monoaldehyde - 2,3,4-trihydroxybenzalde-
hyde (THBA) was used for the first time as a crosslinking agent in CS-
based hydrogels for potential use in tissue engineering applications. It
was hypothesize that the use of a second hydrogel-forming polymer,
namely PC, as well as different functional additives, including calcium-
rich sol-gel-derived BG particles and polyphenolic compounds (RA)
would significantly affect the crosslinking process, and therefore the
properties of CS-based hydrogels. A series of highly porous scaffolds was
evaluated in terms of (i) microstructure and porosity; (ii) mechanical
properties; (iii) thermal properties; (iv) swelling and degradation
behaviour; (v) the in vitro mineralisation process; (vi) antioxidant ac-
tivity; (vii) in vitro cytotoxicity and antiproliferative activity against
normal and cancer human cells.
# 2. Materials and methods
  1. Preparation of the materials
Bioactive glass powder of the following composition (%mol) 54CaO-
40SiO2-6P2O5, denoted as A2, was synthetized using a sol-gel technique
as reported previously (Zagrajczuk et al., 2017). BG was milled in an
attritor with ZrO2 balls in isopropyl alcohol medium to obtain a powder
with a particle size of 1 pm (d50). The particle size distribution and SEM
image of BG are shown in Fig. A.1. Particle size distribution was
measured by laser diffraction Mastersizer-S equipment (Malvern In-
struments, UK) as described previously (Douglas et al., 2019).
Hydrogels were prepared using freeze-drying process. Chitosan
(medium molecular weight; 75-85% deacetylated; Sigma-Aldrich, Ger-
many) and pectin (low esterified amidated pectin from citrus peels;
degree of esterification - 27.4%, degree of amidation - 22.8%, gal-
acturonic acid content - 93.5%; Herbstreith & Fox, Germany) solutions
(2 w/v%) were prepared by dissolving CS and PC powders in 1 v/v%
acetic acid aqueous solution and deionised water, respectively. The pH
values of the polymer solutions were 4.5 and 4.4, respectively. 2,3,4-tri-
hydroxybenzaldehyde (Sigma-Aldrich, Germany) was used as cross-
linking agent. Materials with and without THBA were prepared. THBA,
rosmarinic acid (Carbosynth Ltd., UK), and BG powder was introduced
into materials in the form of 1 w/v% solution/suspension in deionised
water. Adequate solutions/suspensions (CS/PC/THBA/RA/BG) were
mixed (3000 rpm) at room temperature in 2-mL Eppendorf tubes using a
vortexer to obtain materials of compositions presented in Table 1. All
mixtures were filled up to constant volume using 1 v/v% acetic acid. The
scheme showing the order of mixing of the components is shown in
Fig. 1A (if a particular component was not added, the respective mixing
step for that component was omitted). The samples in Eppendorf tubes
were frozen in a laboratory freezer at — 24 °C for 48 h and then freeze-
dried (Alpha 1-4 LSCplus, Christ, Germany, ice condenser tempera-
ture — 55 ° C, vacuum 0.1 mbar) for 48 h.
  1. Microstructure analysis
THBA-free and THBA-containing hydrogels were analysed using
ultra-high resolution scanning electron microscope (SEM) equipped
with a field emission gun and a secondary electron detector (Nova
NanoSEM 200 FEI Europe Company, accelerating voltage 10-15 kV,
spot 4) coupled with an energy dispersion X-ray (EDX) analyser with a
SiLi detector (EDAX, Netherlands) in the low vacuum mode. Cross
2

M. Dziadek et al.
Carbohydrate Polymers 290 (2022) 119486
Table 1
The compositions of materials.
Material	CS (w/w %)	PC (w/w THBA (w/w %) %)	RA (w/w %)	A2 BG (w/ w%)
Uncrosslinked materials
CS	100	-	-	-	-
CS-PC	70	30	-	-	-
CS/A2	100	-	-	-	5
CS-PC/A2	70	30	-	-	5
CS/RA	100	-	-	2	-
CS-PC/RA	70	30	-	2	-
CS/A2/RA	100	-	-	2	5
CS-PC/A2/ 70 RA / Crosslinked materials	30		2	5
CS	100	-	2	-	-
CS-PC	70	30	2	-	-
CS/A2	100	-	2	-	5
CS-PC/A2	70	30	2	-	5
CS/RA	100	-	2	2	-
CS-PC/RA	70	30	2	2	-
CS/A2/RA	100	-	2	2	5
CS-PC/A2/ / RA	70	30	2	2	5

Fig. 1. Scheme showing the order of mixing of the components (if a particular
component was not added, the mixing step for that component was omitted).
sections were prepared by hydrogel cutting with a scalpel blade. Mate-
rials were analysed after coating with a carbon layer.
Architecture of crosslinked hydrogels were evaluated using micro-
computed tomography (p-CT) using a SkyScan 1272 equipment high-
resolution X-ray microtomograph (Bruker Micro-CT, Belgium). 2D pro-
jections were registered averaging 3 frames, rotation of 0.3° and 800 ms
exposure time. The images were registered at a resolution of 4904 x
3280 at an accelerating voltage of 50 kV and a beam current of 200 pA.
The pixel size was fixed at 2 pm.
  1. Mechanical analysis
Mechanical strength of the hydrogels was determined using an
Inspekt 5 Table Blue testing machine (Hegewald & Peschke, Germany)
equipped with a 100 N load cell. Samples were cut into cylinders of 10
mm height and compressed with a displacement rate of 5 mm min-1 (n
= 10). Subsequently, Young's modulus (EC) and the stresses corre-
sponding to compression of a sample by 50% (g5o%) were measured. The
results were expressed as mean ± standard deviation (SD).
  1. Thermal analysis
Thermogravimetric analysis (TGA) was performed using a Discovery
TGA 550 analyser (TA Instruments, USA) in the temperature range from
40 to 600 °C at a heating rate of 10 °C min-1, under a nitrogen
atmosphere. The samples (c.a. 15 mg) were placed in a platinum
crucible.
  1. FTIR analysis
The attenuated total reflection Fourier transform infrared (ATR-
FTIR) spectra were registered using Vertex 70v spectrometer (Bruker,
USA) equipped with a ZnSe ATR crystal. Spectra were collected in the
550-4000 cm-1 spectral range with a resolution of 4 cm-1 and by
averaging 128 scans.
  1. XPS analysis
X-ray photoelectron spectroscopy (XPS) analysis was performed in
an ultrahigh vacuum system (5 • 10-9 mbar) equipped with an SES
R4000 analyser (Gammadata Scienta, Sweden). A monochromatic Al Ka
X-ray source (1486.6 eV) was used. The electron binding energy of C1s
peak was referenced at 284.8 eV. The obtained XPS spectra were ana-
lysed using CasaXPS 2.3.15 software.
  1. Swelling and degradation studies
Swelling and degradation behaviour of hydrogels was investigated
by incubating the samples (n = 5) in phosphate buffered saline (PBS, pH
7.4) at 37 °C. For swelling tests, the samples were weighed at the
beginning of the experiment and again after 3 h, 1, 3, 7, and 14 days of
incubation. Before weighing the samples were placed on filter paper to
remove excess PBS from the surface. Swelling of each sample was
calculated as follows: W‘WW° x 100%, where Wt is weight after specific
period of incubation, W0 is weight before incubation. For degradation
tests, the samples were weighed at the beginning of the experiment and
again after 3, 7, and 14 days of incubation after freeze-drying. Mass loss
of each sample was calculated as follows:	x 100%, where W0 is the
weight of the sample before incubation and Wt is the weight of the
freeze-dried sample after a specific period of incubation. The results
were expressed as mean ± standard deviation (SD).
  1. Antioxidant activity and release of THBA and RA
Antioxidant activity of the hydrogels was evaluated using ABTS and
DPPH free radical scavenging assays and ferric reducing antioxidant
power (FRAP) test (Dziadek, Dziadek, et al., 2021b). The samples were
incubated with shaking in ABTS, DPPH, and FRAP working solutions for
10 min in the dark at 30 °C (n = 3). For ABTS, DPPH, and FRAP assays,
the changes of absorbance at 734 nm, 515 nm, and 593 nm respectively,
were measured using a spectrometer (UV-1800, RayLeigh, China). The
radical scavenging capacity (RSC) of the materials was calculated as
follows: RSC = a°aAs x 100%, where AS was the absorbance of the so-
lution after sample incubation, and A0 was the absorbance of ABTS and
DPPH working solutions. The results of the FRAP test were expressed as
absorbance. The results were expressed as mean ± standard deviation
(SD).
The release of THBA and RA from hydrogels to PBS was evaluated
using HPLC. A Prominence-i LC-2030C 3D Plus system (Shimadzu,
Japan) equipped with a diode array detector (DAD) was used. The
separation was performed on the Luna Omega 5 pm Polar C18, 100 A,
250 x 10 mm column (Phenomenex, California, USA) at 40 °C. The
mobile phase was a mixture of two eluents: A - 0.1% v/v formic acid in
UHQ water and B - 0.1% v/v formic acid in methanol. The flow rate of
the mobile phase was 1.2 mL min-1. The analysis was carried out with
the following gradient conditions: from 20% to 40% B in 10 min, 40% B
for 10 min, from 40% to 50% B in 10 min, from 50% to 60% B in 5 min,
60% B for 5 min, from 60% to 70% B in 5 min, from 70% to 90% B in 5
min, 90% B for 5 min, from 90% to 20% B (the initial condition) in 1 min
and 20% B for 4 min, resulting in a total run time of 60 min. The
3

M. Dziadek et al.
Carbohydrate Polymers 290 (2022) 119486
injection volume was 20 pL. All of the reagents used for HPLC analysis
were purchased from Sigma-Aldrich, Germany.
  1. In vitro mineralisation studies
The mineralisation process of hydrogels was performed by incuba-
tion in simulated body fluid (SBF), prepared according to Kokubo and
Takadama (2006). Samples were incubated in SBF for 7 and 14 days at
37 °C, freeze-dried and analysed using SEM/EDX and ATR-FTIR
methods as mentioned above.
  1. In vitro cell studies
The human normal skin fibroblasts (BJ, ATCC, USA) and the human
colon cancer epithelial cells (HT-29, ATCC, USA) were cultured in direct
contact with crosslinked materials in Eagle's Minimum Essential Me-
dium (EMEM, Sigma-Aldrich, MO, USA) and McCoy's 5a Medium
Modified (ATCC, USA), respectively, both containing 10% Fetal Bovine
Serum (FBS) at a density of 2-104 cells/mL/well for 1, 3, 7, and 10 days
in 48-well plates. The bottom surfaces of tissue culture polystyrene
(TCPS) wells served as a control. The proliferation rate of cells and
cytotoxicity of hydrogels were assessed using the ToxiLight™ BioAssay
Kit and ToxiLight™ 100% Lysis Reagent Set (Lonza, USA) according to
the manufacturer's protocol. The kit was used to quantify adenylate ki-
nase in both supernatant (representing damaged cells) and lysate (rep-
resenting intact adherent cells). The results were expressed as mean ±
standard deviation (SD) from 4 samples for each experimental group.
  1. Statistical analysis
The results were analysed using one-way analysis of variance
(ANOVA) with Duncan post hoc tests, which were performed with Sta-
tistica 13 (StatSoft®, USA) software. The results were considered sta-
tistically significant when p < 0.05.
# 3. Results and discussion
The use of monoaldehydes as crosslinking agents of chitosan is not as
common as the use of other ones, e.g. glutaraldehyde. However, due to
their natural origin, low cytotoxicity, low costs, and therapeutic activity,
they have attracted great attention for crosslinking chitosan hydrogels
for biomedical applications. To date, the following monoaldehydes have
been used - vanillin (Hu et al., 2021; Karakurt et al., 2021; Xu et al.,
, salicylaldehyde (Iftime et al., 2020, 2017), nitrosalicylaldehyde
(Craciun et al., 2019; Olaru et al., 2018), and cinnamaldehyde (Marin
et al., 2014). In most cases, single-component hydrogels were obtained.
However, there are only a few reports on the introduction of functional
components into imine-chitosan hydrogels and examination of their
effect on the crosslinking process, and thus the final properties of ma-
terials. In recent works, melt-derived bioactive glass particles (Hu et al.,
2021) and diclofenac sodium salt (Craciun et al., 2019; Iftime et al.,
2020), as a model drug, were used. In the present study we developed
multicomponent chitosan-based hydrogels modified with a second
hydrogel-forming polymer - pectin, as well as different functional ad-
ditives - bioactive glass particles and rosmarinic acid. For systematic
evaluation of the obtained hydrogels, the additives were introduced
alone or in combination to both materials prepared in the presence and
absence of monoaldehyde (THBA, pyrogallolaldehyde). It is worth
mentioning that the THBA molecule contains three hydroxyl groups
which, in addition to their ability to stabilize the imine bond, provided
additional binding sides for the chains of both polymers and other
components. Importantly, these three hydroxyl groups impart antioxi-
dant properties to the THBA. Pectin was able to form polyelectrolyte
complexes with chitosan through electrostatic interactions between
ionised moieties. The BG particles used, similarly to RA, also contain
numerous hydroxyl groups capable of forming hydrogen bonds.
Furthermore, calcium ions, massively released from BG particles, were
involved in ionic crosslinking of pectin. All of these reactions and in-
teractions provided a multi-level crosslinking effect of chitosan-based
hydrogels, as was schematically illustrated in Fig. 2, affecting their
properties discussed in the next subsections.
Microstructure analysis
SEM analysis of hydrogels revealed irregular highly porous
morphology characteristic of biopolymer-based porous materials ob-
tained using freeze-drying processes (Fig. 3) (Coimbra et al., 2011; Luppi
et al., 2010). All materials showed sheet/sponge-like structures. Addi-
tionally, the hydrogels with pectin contained fibrous-like structures,
observed also by Coimbra et al., 2011 and Luppi et al., 2010 in CS-PC
porous materials. Pores of crosslinked materials seemed be smaller
compared to uncrosslinked hydrogels. This may be due to lower
amounts of water entrapped between crosslinked chitosan chains (Iftime
et al., 2017), which was confirmed by TG analysis (Fig. A.4). Although
BG particles are not clearly visible in SEM and pCT analyses, the main
components of BG (Si, Ca) were detected using EDX analysis, confirming
their presence in the hydrogel matrices. This may be related to the low
concentration of BG particles in materials (5 w/w%) and their highly
homogeneous distribution with no tendency to agglomerate.
pCT analysis of crosslinked hydrogels proved nearly 100% inter-
connectivity of the pores and high porosity, regardless of the composi-
tion of the hydrogels. Open porosity was in the range of 94.9%-96.5%
(Fig. 3). The analysis of pore size distribution showed that all hydrogels
had pores predominantly in the range of 50-150 pm (Fig. 4A), which is
consistent with SEM observations (Fig. 3). Smaller (2-50 pm) and larger
(>150 pm) pores were also present, as depicted by Fig. 4A. Such multi-
scale pore size distribution, high porosity and interconnectivity promote
migration and proliferation of osteogenic cells, vascularization, trans-
port of nutrients and waste, as well as bone tissue ingrowth (Iviglia et al.,
. Wall thickness was predominantly in the range of 2-18 pm
(Fig. 4B). 3D reconstructions and cross sections obtained from pCT
analysis revealed that CS-based materials had homogenous porous
morphology. In the case of CS-PC-based hydrogels, two phases differing
in microstructure were observed. Within the most porous phase, similar
to that observed in CS-based materials, an inhomogenously distributed
and significantly less porous second phase was noted. The latter was
possibly PC and/or PC-CS PEC. Inhomogeneous distribution of the PC-
containing phase probably results from immediate electrostatic in-
teractions between pectin and chitosan during material preparation.
This may also explain the lack of aforementioned agglomeration of BG.
This was in contrast to our previous observations made for injectable
PC/BG hydrogels, in which non-uniformly distributed agglomerates of
A2 BG particles were noted, as a result of extremely rapid local cross-
linking process of pectin induced by Ca2+ ions released from BG
(Douglas et al., 2019). It should be pointed out that during hydrogel
preparation, PC solution was added after mixing BG suspension with
chitosan solution. As both calcium-induced crosslinking of pectin and
formation of PEC are competitive processes, the order in which the
components were mixed favours the latter process, preventing BG
agglomeration.
To date, pCT techniques have been used to investigate hydrogel
microstructure and distribution of inorganic particles in hydrogel
matrices (Douglas et al., 2019; Dziadek et al., 2019; Dziadek, Charuza,
et al., 2021a). However, our results clearly indicate that pCT imaging is
also useful tool to study homogeneity and interactions in hydrogel
polyelectrolyte complex matrices formed between polyanions and pol-
ycations, i.e. chitosan and pectin.
Mechanical analysis
As shown in Fig. 4C, hydrogels crosslinked with THBA exhibited
significantly higher values of Ec and g50% (0.22-1.60 MPa and 78-158
4

M. Dziadek et al.
Carbohydrate Polymers 290 (2022) 119486
particles
о Ca2+ ions
o RA
+ Wv(D electrostatic interaction
hydrogen bond
Fig. 2. Schematic illustration of the network of THBA-containing CS-PC/A2/RA hydrogel.
kPa, respectively) compared to materials without THBA (0.07-0.73 MPa
and 63-123 kPa, respectively). In turn, the presence of pectin in both
THBA-containing and THBA-free materials led to significant increases in
Ec and g50% (0.64-1.60 MPa and 106-158 kPa, respectively), when
comparing to materials without PC (0.07-0.48 MPa and 63-113 kPa,
respectively). Interestingly, improved mechanical properties were
observed despite an uneven distribution of the PC-containing phase.
However, because of its lower porosity, this phase may be considered as
a reinforcing element of a highly porous hydrogel matrix. In the group of
materials crosslinked with THBA, the presence of each additive resulted
in higher values of both parameters tested. However, the highest Ec
values were showed by CS-PC-based hydrogels modified with RA (CS-
PC/RA, 1.56 MPa) as well as with both RA and BG (CS-PC/A2/RA, 1.60
MPa), while the highest g50% value was noted for the first mentioned one
(CS-PC/RA, 158 kPa).
Crosslinking has been shown to be an effective strategy to enhance
the mechanical properties of biopolymers as a result of formation of a
three-dimensional polymer network (Martinez et al., 2015). Xu et al.,
2018 showed that the formation of Schiff base bond/hydrogen bond
linkage in chitosan hydrogels crosslinked with vanillin provide good
mechanical strength and additional self-healing properties. The effect of
interactions occurring between chitosan and pectin chains (electrostatic,
ion-dipole interactions and hydrogen bonding) on improvement of me-
chanical properties of porous CS/PC materials was previously observed
(Demir et al., 2020). In turn, Chen et al., 2010 showed that the presence
of Ca2+ ions in a CS-PC PEC membrane significantly improved its tensile
strength, because of additional calcium-mediated ionic interactions
between pectin chains. In recent work, BG particles were considered as a
co-crosslinker, improving mechanical behaviour of CS/BG/vanillin
hydrogels. BG particles provided additional binding sites between chi-
tosan and vanillin through multiple hydrogen bonding (Hu et al., 2021).
Taking together, the improved mechanical properties of the obtained
multicomponent scaffolds could be attributed to the higher crosslinking
degree promoted by multifaceted interactions between components.
Formation of the Schiff base in the chitosan matrix was confirmed by
development of a distinct yellow colour (Fig. 5C) (Stroescu et al., 2015).
The FTIR spectra of THBS-containing hydrogels showed an absorption
band at 1628 cm-1, which may be attributed to the stretching vibration
of imine bonding (Fig. A.2). Furthermore, an absorption band of the
phenolic hydroxyl groups of THBA shifted from 1279 to 1268 cm-1,
which may be due to the H-bonding between THBA and other compo-
nents (Y. Zhang et al., 2014). The high-resolution C1s and N1s XPS
spectra of the THBA-containing CS hydrogel revealed peaks at 288.8 eV
and 398.8 eV (Fig. A.3), respectively, which can be assigned to the
binding energy of the C-N bond (Gao et al., 2021), suggesting that a
Schiff base reaction occurred. When analysing the TG curves, cross-
linked materials showed lower water content (lower initial weight loss
up to 200 ° C) as well as enhanced thermal stability (higher temperature
of thermal decomposition, occurring between 200 and 350 °C, and
higher residual weight) compared to uncrosslinked hydrogels, con-
firming the presence of covalent Schiff base bonding (Fig. A.4) (Mon-
taser et al., 2019). Moreover, in the case of uncrosslinked materials,
temperature of thermal decomposition of CS-PC hydrogels tended to be
higher compared to CS materials, which may indicate ionic interactions
between both polymers (Martins et al., 2018).
5

M. Dziadek et al.
Carbohydrate Polymers 290 (2022) 119486
Fig. 3. Representative SEM images and EDX spectra of the THBA-free and THBA-containing hydrogels. Representative pCT analyses of the crosslinked hydrogels - 3D
reconstructions, cross sections, and open porosity (OP).
Swelling and degradation studies
Swelling and degradation behaviour of hydrogels crosslinked with
THBA was investigated, because only these ones were able to maintain a
sufficient integrity for accurate weighing (Fig. 5C). Materials swelled the
most after the first 3 h of incubation in PBS (1878-4287%). Swelling
ability of all THBA-containing materials gradually increased with
increasing incubation time until day 7 (Fig. 5A). After 14 days of incu-
bation, a decrease in swelling was observed, which suggests that the
dissolution process was accelerated. This is in agreement with the
highest mass loss of hydrogels after 14-day incubation (Fig. 5B).
Hydrogels containing RA and CS-PC/A2 material exhibited a lower
decrease in swelling and lower mass loss after 14-day incubation
compared to other materials. Furthermore, significantly lower water
uptake and mass loss over the entire incubation period were observed
for these materials. When comparing hydrogels with pectin, those ones
modified with BG particles showed significantly reduced swelling and
degradation. Importantly, materials combining all components (CS, PC,
THBA, RA, BG) were the most stable.
Macroscopic observations showed that the materials crosslinked
with THBA maintained shape and integrity over the entire incubation
period. The THBA-free hydrogels containing pectin did not dissolve
completely during 14-day incubation in PBS, in contrast to materials
without this component (Fig. 5C). Also, hydrogels with RA exhibited
incomplete dissolution in PBS, however debris were much smaller after
14-day incubation compared to materials with PC. THBA-free CS-PC/
6

M. Dziadek et al.
Carbohydrate Polymers 290 (2022) 119486
Fig. 4. Quantitative data based on pCT analyses of the THBA-containing
hydrogels: pore size distribution (A) and structure size distribution (B).
Compression test results: Young’s modulus and stresses corresponding to
compression of a sample by 50% of the THBA-free and THBA-containing
hydrogels (C). Statistically significant differences (p < 0.05) between mate-
rials are indicated by subsequent lower (EC) and upper (o50%) Latin letters.
Different letters indicate statistically significant differences.
A2/RA hydrogel showed the lowest tendency to disintegrate/dissolve
with a very high swelling rate.
Both swelling and degradation behaviour of hydrogels strongly
depend on the degree of crosslinking and also the nature of linkage. In
general, the higher the crosslinking degree, the lower the swelling
ability and the slower the degradation rate (Hu et al., 2021; Iftime et al.,
. Therefore, the results clearly indicated that THBA was success-
fully used as a crosslinking agent of CS-based hydrogels. The presence of
PC, RA, and BG in THBA-free materials also induced crosslinking, but
this effect was much weaker. This was due to the fact that the covalent
bonding (Schiff base bond) is known to be much stronger than ionic
interactions (calcium-mediated interactions between PC chains and in-
teractions between ionised functional groups of CS and PC) as well as
hydrogen bonding (e.g. between hydroxyl groups of RA, BG, CS, and PC).
The introduction of PC, RA, and BG into THBA-containing hydrogels
gave a synergistic crosslinking effect.
Pornpimon and Sakamon (2010) showed that swelling of the chito-
san films was reduced upon modification with the plant extract rich in
polyphenols, as a result of intermolecular interactions between chitosan
and the extract components. In contrast, literature data showed that the
swelling ability and degradation rate of CS-based materials crosslinked
with glutaraldehyde considerably increased upon addition of PC (Demir
et al., 2020), while the presence of Ca2+ ions in CS-PC PEC materials
accelerated the weight loss during incubation in PBS (Chen et al., 2010).
It seems that THBA provided a stabilizing effect in CS-PC hydrogels, due
to the hydrogen bonds established between the hydroxyl groups of
THBA and pectin moieties. Furthermore, because of the lower content of
pectin with respect to chitosan, PC-containing phase may be entrapped
between highly crosslinked CS phases, creating a protective environ-
ment against water. This can be supported by pCT analysis (Fig. 3).
Antioxidant activity and release of biologically active compounds
The radical scavenging capacity (RSC) against the ABTS^+ and DPPH
radicals, as well as the ferric reducing antioxidant potential (FRAP) of
the hydrogels, are shown in Fig. 6A. Antioxidant activity of hydrogels
can be clearly ascribed to the presence of phenolic components - THBA
and RA. The materials containing these components showed high RSC
and reducing potential which increased in the following order:
THBA<RA<THBA+RA. In the case of materials with both THBA and RA,
antioxidant potential did not depend on composition, in contrast to
hydrogels with a single phenolic component (THBA or RA).
The release of biologically active compounds form hydrogels was
evaluated after 14-day incubation in PBS (Fig. 6B). The release of THBA
and RA form hydrogels crosslinked with THBA was below 1% of the
initial content in the materials (data not shown). In the case of THBA-
free hydrogels, release of RA was in the range 21%-32%, depending
on material composition. The presence of PC and BG separately
decreased RA release significantly, while combination of these compo-
nents (PC and BG) reduced RA release to the greatest extent. The release
of RA from THBA-free hydrogels corresponded to yellowish colour of
incubation medium (Fig. 5C).
A very low release level of THBA from THBA-containing hydrogels
indicated its strong interactions with other components of the materials,
confirming contribution in crosslinking process. Crosslinking with THBA
inhibited almost completely the release of RA. In the case of THBA-free
materials, RA release level corresponded with swelling/dissolution rate
of the hydrogels (evaluated macroscopically - Fig. 5C). This indicates
that, besides the interaction of RA with hydrogel components, the
crosslinking process using THBA enables RA to be effectively entrapped
in the hydrogel network. This is in agreement with other studies indi-
cating that reduced release of biologically active components from the
hydrogel is closely correlated with a higher degree of crosslinking and
therefore lower swelling and degradation rates (Iftime et al., 2020;
Karakurt et al., 2021).
Although THBA and RA were practically not released from the
7

M. Dziadek et al.
Carbohydrate Polymers 290 (2022) 119486
Fig. 5. Swelling (A) and mass loss (B) of the THBA-containing hydrogels. Statistically significant differences (p < 0.05) between materials are indicated by sub-
sequent lower (3 h), upper (1 day) Latin letters, Greek letters (3 days), Arabic numerals (7 days), and Roman numerals (14 days). Different letters/numerals indicate
statistically significant differences. Macroscopic images of the THBA-free and THBA-containing hydrogels before (as prepared) and after 14-day incubation in
PBS (C).
hydrogels crosslinked with THBA, they showed high antioxidant activ-
ity. Furthermore, the release level of RA from THBA-free hydrogels did
not correlate with RSC and reducing potential. This may indicate that
antioxidant activity of hydrogels is mainly attributed to antioxidants
attached to the materials, not to the released ones (Dziadek, Dziadek,
et al., 2021b). Some differences in antioxidant activity between hydro-
gels containing a single phenolic compound (THBA or RA) may result
from different interactions between them and other components (CS, PC,
BG). As the antioxidant activity of a phenolic compound depends on the
total number of phenolic hydroxyl groups able to interact with reactive
oxygen species by donating hydrogens, phenolic hydroxyl groups
involved in hydrogen bonding were not available to scavenge free rad-
icals/reduce ferric ions. In turn, the combination of both THBA and RA
provided maximal antioxidant effect.
In vitro mineralisation studies
Mineralisation process of the THBA-containing hydrogels after in-
cubation in SBF was assessed using SEM/EDX and ATR-FTIR methods
(Fig. 7). After 14-day incubation, hydrogels containing BG particles
were covered with a uniform layer rich in calcium (Ca) and phosphorus
(P). Furthermore, quite large amounts of sodium (Na), chlorine (Cl), and
potassium (K) were incorporated into materials from SBF. In the case of
crosslinked hydrogels without BG, only the latter elements (Na, Cl, K)
were detected after incubation (data not shown). ATR-FTIR spectra of
hydrogels containing BG particles incubated in SBF releveled new bands
proving mineralisation by a CaP phase. Furthermore, the reduction in
the intensity of bands arising from hydrogels was observed, indicating
that the layer was thick and uniformly covered the materials. The bands
noted in the ranges of 960-1130 cm~1 and 600-560 cm~1 correspond to
stretching and bending vibrations of PO43~ groups in crystalline CaP,
respectively (Bossard et al., 2019). The bands in spectra of hydrogels
containing RA tended to be sharper, compared to those without RA,
suggesting the presence of CaP phase with higher crystallinity. This may
be due to acceleration of CaP layer crystallization by additional poly-
phenolic compound with numerous phenolic hydroxyl groups capable to
interact with Ca2+ ions from SBF (Zhou et al., 2012). There were no
significant changes in the spectra of THBA-containing hydrogels without
BG after incubation, confirming SEM/EDX analysis.
These results confirmed the mineralisation ability of CS- and CS-PC-
based hydrogels containing BG particles. This may provide chemical
bonding with bone, as well as improved mechanical properties of the
8

M. Dziadek et al.
Carbohydrate Polymers 290 (2022) 119486
Fig. 6. Radical scavenging capacity (RSC) against the ABTS*+ and DPPH* radicals, as well as ferric reducing antioxidant potential (FRAP) of the THBA-free and
THBA-containing hydrogels (A). Statistically significant differences (p < 0.05) are indicated by subsequent lower (ABTS), upper (DPPH) Latin letters and Greek letters
(FRAP). The release of RA to PBS after 14-day incubation - % of the initial content in the materials (B). Statistically significant differences (p < 0.05) are indicated by
subsequent lower Latin letters. Different letters indicate statistically significant differences.
Fig. 7. SEM images, EDX spectra, and ATR-FTIR spectra of the THBA-containing hydrogels after 14-day incubation in SBF.
hydrogels after implantation, actively promoting bone regeneration
(Mota et al., 2012).
In vitro cell studies
Cytotoxicity and antiproliferative activity of THBA-containing
hydrogels were evaluated on normal fibroblast cells and colon cancer
cells (Fig. 8). The number of normal cells in contact with tested materials
was lower after each cell culture period compared to the control (TCPS).
Nevertheless, the fibroblasts cultured on hydrogels showed a high pro-
liferation rate. After 10 days of culture, there were no statistically sig-
nificant difference between materials. In the case of cancer cells, a
9

M. Dziadek et al.
Carbohydrate Polymers 290 (2022) 119486
Fig. 8. The response of BJ human normal skin fibroblasts and HT-29 human colon cancer epithelial cells cultured in contact with THBA-containing hydrogels:
adenylate kinase (AK) level in the lysate corresponding to the number of intact adherent cells (A), AK level in the supernatant representing material cytotoxicity (B).
Statistically significant differences (p < 0.05) between materials and TCPS are indicated by subsequent lower (1 day), upper (3 days) Latin letters, Greek letters (7
days), Arabic numerals (10 days). Different letters indicate statistically significant differences.
strong antiproliferative activity of the materials was noted. The number
of cancer cells in contact with the hydrogels was several times lower
compared to TCPS and decreased with increasing culture time. In the
case of materials containing RA, a significantly lower number of cells
was observed after 3 days of culture, compared to hydrogels without RA.
In turn, after 10-day culture, the number of cells in contact with mate-
rials did not differ significantly. Release of adenylate kinase from both
normal and cancer cells in contact with hydrogels was on the same level
or even lower compared to the control, indicating a low cytotoxic effect.
Materials containing RA showed lower cytotoxicity when compared to
unmodified ones.
The results showed that materials crosslinked with THBA were not
cytotoxic against normal and cancer cells, however they inhibited the
proliferation of cancer cells, possibly indicating a modulation of the cell
cycle. This suggested that apoptosis rather than necrosis was a pathway
for cancer cell death. Inducing apoptosis of cancer cells while reducing
the death of normal cells is one of the most desirable mechanisms of
action of anticancer therapies (Kwan et al., 2015). Antiproliferative
activity of THBA-containing hydrogels may be ascribed to the presence
of phenolic compounds - THBA and RA. As mentioned above, mono-
aldehydes, such as vanillin (Karakurt et al., 2021), salicylaldehyde
(Iftime et al., 2017), o-vanillin, and 2,4,6-trihydroxybenzaldehyde
(Marton et al., 2016), as well as polyphenols, for instance RA (Swamy
et al., 2018), exhibited antitumor activity against different types of
cancer cells. Similarly to antioxidant properties, anticancer activity was
possibly attributed mainly to compounds attached to materials.
# 4. Conclusions
In the present work, a series of highly porous chitosan-based
hydrogels was prepared and comprehensively evaluated. A simple and
green method for crosslinking with the use of monoaldehyde - 2,3,4-tri-
hydroxybenzaldehyde was successfully applied. The hydrogels were
modified with a second hydrogel-forming polymer - pectin, as well as
different functional additives - bioactive glass particles and rosmarinic
acid. All of these were involved in the crosslinking process of the
hydrogels, while simultaneously modulating their properties or
imparting completely new ones. The crosslinking process with THBA
resulted in significantly improved mechanical properties, high swelling
capacity and delayed degradation. In addition to the crosslinking func-
tion, THBA provided high antioxidant activity and also a selective
antiproliferative effect on cancer cells with no cytotoxicity for normal
cells. Hydrogels containing pectin showed significantly modified
microstructure and enhanced mechanical strength, while the combina-
tion with bioactive glass particles gave improved stability in PBS. All
hydrogels modified with bioactive glass particles exhibited the ability to
mineralise in SBF. The addition of rosmarinic acid enhanced antioxidant
and anticancer activities as well as promoting the mineralisation pro-
cess. The results indicated that the obtained hydrogels represent
promising multifunctional biomaterials with a wide range of tunable
10

M. Dziadek et al.
Carbohydrate Polymers 290 (2022) 119486
physicochemical and biological properties with great potential for the
use in different tissue engineering fields, for instance in bone regener-
ation or after tumour resection.
# CRediT authorship contribution statement
Michal Dziadek: Conceptualization, Methodology, Investigation,
Writing - original draft, Writing - review & editing, Visualization, Su-
pervision, Project administration, Funding acquisition. Kinga Dziadek:
Conceptualization, Methodology, Investigation, Visualization, Writing -
original draft. Szymon Salagierski: Investigation, Visualization,
Writing - original draft. Mariola Drozdowska: Investigation, Visuali-
zation, Writing - original draft. Andrada Serafim: Investigation, Visu-
alization, Writing - original draft, Funding acquisition. Izabela-Cristina
Stancu: Investigation, Visualization, Writing - original draft, Funding
acquisition. Piotr Szatkowski: Investigation, Visualization, Writing -
original draft, Funding acquisition. Aneta Kopec: Writing - review &
editing, Supervision. Izabella Rajzer: Writing - review & editing, Su-
pervision. Timothy E.L. Douglas: Writing - review & editing, Super-
vision. Katarzyna Cholewa-Kowalska: Writing - review & editing,
Supervision, Funding acquisition.
# Declaration of competing interest
The authors declare that they have no known competing financial
interests or personal relationships that could have appeared to influence
the work reported in this paper.
# Acknowledgments
This work was supported by the National Science Centre, Poland,
grant nos. 2017/27/B/ST8/00195 (KCK) and 2019/32/C/ST5/00386
(MD). The pCT investigations were possible due to European Regional
Development Fund through Competitiveness Operational Program
2014-2020, Priority axis 1, ID P_36_611, MySMIS code 107066, INO-
VABIOMED (AS, ICS). This work was partly supported by program
“Excellence initiative - research university” for the AGH University of
Science and Technology. The authors thank Herbstreith & Fox Company
(Germany) for delivering pectin.
# Appendix A. Supplementary data
Supplementary data to this article can be found online at https://doi.
org/10.1016/j.carbpol.2022.119486.
# References
Birch, N. P., Barney, L. E., Pandres, E., Peyton, S. R., & Schiffman, J. D. (2015). Thermal-
responsive behavior of a cell compatible chitosan/pectin hydrogel.
Biomacromolecules, 16(6), 1837-1843. https://doi.org/10.1021/ACS.
BIOMAC.5B00425
Bossard, C., Granel, H., Jallot, E., Montouillout, V., Fayon, F., Soulie, J., ... Lao, J.
(2019). Mechanism of calcium incorporation inside sol-gel silicate bioactive glass
and the advantage of using Ca(OH)2 over other calcium sources. ACS Biomaterials
Science & Engineering, 5(11), 5906-5915. https://doi.org/10.1021/
ACSBIOMATERIALS.9B01245
Chen, P. H., Kuo, T. Y., Kuo, J. Y., Tseng, Y. P., Wang, D. M., Lai, J. Y., & Hsieh, H. J.
(2010). Novel chitosan-pectin composite membranes with enhanced strength,
hydrophilicity and controllable disintegration. Carbohydrate Polymers, 82(4),
1236-1242. https://doi.org/10.1016/J.CARBPOL.2010.06.057
Coimbra, P., Ferreira, P., de Sousa, H. C., Batista, P., Rodrigues, M. A., Correia, I. J., &
Gil, M. H. (2011). Preparation and chemical and biological characterization of a
pectin/chitosan polyelectrolyte complex scaffold for possible bone tissue
engineering applications. International Journal of Biological Macromolecules, 48(1),
112-118. https://doi.org/10.1016/J.IJBIOMAC.2010.10.006
Craciun, A. M., Mititelu Tartau, L., Pinteala, M., & Marin, L. (2019). Nitrosalicyl-imine-
chitosan hydrogels based drug delivery systems for long term sustained release in
local therapy. Journal of Colloid and Interface Science, 536, 196-207. https://doi.org/
10.1016/J.JCIS.2018.10.048
Cui, S., Yao, B., Gao, M., Sun, X., Gou, D., Hu, J., ... Liu, Y. (2017). Effects of pectin
structure and crosslinking method on the properties of crosslinked pectin nanofibers.
Carbohydrate Polymers, 157, 766-774. https://doi.org/10.1016/J.
CARBPOL.2016.10.052
Demir, D., Ceylan, S., Göktürk, D., & Bölgen, N. (2020). Extraction of pectin from albedo
of lemon peels for preparation of tissue engineering scaffolds. Polymer Bulletin 2020
78:4, 78(4), 2211-2226. https://doi.org/10.1007/S00289-020-03208-1
Douglas, T. E. L., Kumari, S., Dziadek, K., Dziadek, M., Abalymov, A., Cools, P., .
Skirtach, A. G. (2017). Titanium surface functionalization with coatings of chitosan
and polyphenol-rich plant extracts. Materials Letters, 196, 213-216. https://doi.org/
10.1016/J.MATLET.2017.03.065
Douglas, T. E. L., Dziadek, M., Schietse, J., Boone, M., Declercq, H. A., Coenye, T., ...
Skirtach, A. G. (2019). Pectin-bioactive glass self-gelling, injectable composites with
high antibacterial activity. Carbohydrate Polymers, 205, 427-436. https://doi.org/
10.1016/J.CARBPOL.2018.10.061
Dziadek, M., Kudlackova, R., Zima, A., Slosarczyk, A., Ziabka, M., Jelen, P., ...
Douglas, T. E. L. (2019). Novel multicomponent organic-inorganic WPI/gelatin/CaP
hydrogel composites for bone tissue engineering. Journal of Biomedical Materials
Research Part A, 107(11), 2479-2491. https://doi.org/10.1002/JBM.A.36754
Dziadek, M., Charuza, K., Kudlackova, R., Aveyard, J., D’Sa, R., Serafim, A., ...
Douglas, T. E. L. (2021a). Modification of heat-induced whey protein isolate
hydrogel with highly bioactive glass particles results in promising biomaterial for
bone tissue engineering. Materials & Design, 205, 109749. https://doi.org/10.1016/
J.MATDES.2021.109749
Dziadek, M., Dziadek, K., Checinska, K., Zagrajczuk, B., Golda-Cepa, M., Brzychczy-
Wloch, M., . Cholewa-Kowalska, K. (2021b). PCL and PCL/bioactive glass
biomaterials as carriers for biologically active polyphenolic compounds:
Comprehensive physicochemical and biological evaluation. Bioactive Materials, 6(6),
1811-1826. https://doi.org/10.1016/J.BIOACTMAT.2020.11.025
Gao, C., Wang, S., Liu, B., Yao, S., Dai, Y., Zhou, L., Qin, C., & Fatehi, P. (2021).
Sustainable Chitosan-Dialdehyde Cellulose Nanocrystal Film. Materials 2021, Vol.
14, Page 5851, 14(19), 5851. https://doi.org/10.3390/MA14195851.
Hu, J., Wang, Z., Miszuk, J. M., Zhu, M., Lansakara, T. I., Tivanski, A.v., . Sun, H.
(2021). Vanillin-bioglass cross-linked 3D porous chitosan scaffolds with strong
osteopromotive and antibacterial abilities for bone tissue engineering. Carbohydrate
Polymers, 271, 118440. https://doi.org/10.1016/J.CARBPOL.2021.118440
Iftime, M. M., Morariu, S., & Marin, L. (2017). Salicyl-imine-chitosan hydrogels:
Supramolecular architecturing as a crosslinking method toward multifunctional
hydrogels. Carbohydrate Polymers, 165, 39-50. https://doi.org/10.1016/J.
CARBPOL.2017.02.027
Iftime, M. M., Mititelu Tartau, L., & Marin, L. (2020). New formulations based on salicyl-
imine-chitosan hydrogels for prolonged drug release. International Journal of
Biological Macromolecules, 160, 398-408. https://doi.org/10.1016/J.
IJBIOMAC.2020.05.207
Iviglia, G., Cassinelli, C., Bollati, D., Baino, F., Torre, E., Morra, M., & Vitale-
Brovarone, C. (2016). Engineered porous scaffolds for periprosthetic infection
prevention. Materials Science and Engineering: C, 68, 701-715. https://doi.org/
10.1016/J.MSEC.2016.06.050
Karakurt, I., Ozaltin, K., Vargun, E., Kucerova, L., Suly, P., Harea, E., ... Mozetic, M.
(2021). Controlled release of enrofloxacin by vanillin-crosslinked chitosan-polyvinyl
alcohol blends. Materials Science and Engineering: C, 126, 112125. https://doi.org/
10.1016/J.MSEC.2021.112125
Kokubo, T., & Takadama, H. (2006). How useful is SBF in predicting in vivo bone
bioactivity? Biomaterials, 27(15), 2907-2915. https://doi.org/10.1016/J.
BIOMATERIALS.2006.01.017
Kuhlmann, A., & Röhl, C. (2008). Phenolic Antioxidant Compounds Produced by in
Vitro. Cultures of Rosemary (Rosmarinus officinalis.) and Their Anti-inflammatory
Effect on Lipopolysaccharide-Activated Microglia. Http://Dx.Doi.Org/10.1080
/13880200600794063, 44(6), 401-410. https://doi.org/10.1080/13880200600
794063.
Kwan, Y. P., Saito, T., Ibrahim, D., Al-Hassan, F. M. S., Oon, C. E., Chen, Y., Jothy, S. L.,
Kanwar, J. R., & Sasidharan, S. (2015). Evaluation of the cytotoxicity, cell-cycle
arrest, and apoptotic induction by Euphorbia hirta in MCF-7 breast cancer cells.
https://doi.org/10.3109/13880209.2015.1064451, 54(7), 1223-1236. https://doi.
org/10.3109/13880209.2015.1064451.
Lee, J.-W., Asai, M., Jeon, S.-K., Iimura, T., Yonezawa, T., Cha, B.-Y., ... Yamaguchi, A.
(2015). Rosmarinic acid exerts an antiosteoporotic effect in the RANKL-induced
mouse model of bone loss by promotion of osteoblastic differentiation and inhibition
of osteoclastic differentiation. Molecular Nutrition & Food Research, 59(3), 386-400.
https://doi.org/10.1002/MNFR.201400164
Li, J., Zhu, D., Yin, J., Liu, Y., Yao, F., & Yao, K. (2010). Formation of nano-
hydroxyapatite crystal in situ in chitosan-pectin polyelectrolyte complex network.
Materials Science and Engineering: C, 30(6), 795-803. https://doi.org/10.1016/J.
MSEC.2010.03.011
Luppi, B., Bigucci, F., Abruzzo, A., Corace, G., Cerchiara, T., & Zecchi, V. (2010). Freeze-
dried chitosan/pectin nasal inserts for antipsychotic drug delivery. European Journal
of Pharmaceutics and Biopharmaceutics, 75(3), 381-387. https://doi.org/10.1016/J.
EJPB.2010.04.013
Maciel, V. B. V., Yoshida, C. M. P., & Franco, T. T. (2015). Chitosan/pectin
polyelectrolyte complex as a pH indicator. Carbohydrate Polymers, 132, 537-545.
https://doi.org/10.1016/J.CARBPOL.2015.06.047
Mallick, S. P., Suman, D. K., Singh, B. N., Srivastava, P., Siddiqui, N., Yella, V. R.,
Madhual, A., & Vemuri, P. K. (2020). Strategies toward development of
biodegradable hydrogels for biomedical applications. https://doi.org/10.1080/25
740881.2020.1719135, 59(9), 911-927. https://doi.org/10.1080/25740881.202
0.1719135.
Marin, L., Moraru, S., Popescu, M. C., Nicolescu, A., Zgardan, C., Simionescu, B. C., &
Barboiu, M. (2014). Out-of-water constitutional self-organization of
11

M. Dziadek et al.
Carbohydrate Polymers 290 (2022) 119486
chitosan-Cinnamaldehyde dynagels. Chemistry - A European Journal, 20(16),
4814-4821. https://doi.org/10.1002/CHEM.201304714
Martinez, A., Blanco, M. D., Davidenko, N., & Cameron, R. E. (2015). Tailoring chitosan/
collagen scaffolds for tissue engineering: Effect of composition and different
crosslinking agents on scaffold properties. Carbohydrate Polymers, 132, 606-619.
https://doi.org/10.1016/J.CARBPOL.2015.06.084
Martins, J. G., de Oliveira, A. C., Garcia, P. S., Kipper, M. J., & Martins, A. F. (2018).
Durable pectin/chitosan membranes with self-assembling, water resistance and
enhanced mechanical properties. Carbohydrate Polymers, 188, 136-142. https://doi.
org/10.1016/J.CARBPOL.2018.01.112
Marton, A., Kusz, E., Kolozsi, C., Tubak, V., Zagotto, G., Buzas, K., Quintieri, L., &
Vizler, C. (2016). Vanillin analogues o-vanillin and 2,4,6-trihydroxybenzaldehyde
inhibit NFkB activation and suppress growth of A375 human melanoma. Anticancer
Research, 36(11), 5743-5750. https://doi.org/10.21873/anticanres.11157.
Montaser, A. S., Wassel, A. R., & Al-Shaye’a, O. N. (2019). Synthesis, characterization
and antimicrobial activity of Schiff bases from chitosan and salicylaldehyde/TiO2
nanocomposite membrane. International Journal of Biological Macromolecules, 124,
802-809. https://doi.org/10.1016/J.IJBIOMAC.2018.11.229
Mota, J., Yu, N., Caridade, S. G., Luz, G. M., Gomes, M. E., Reis, R. L., . Mano, J. F.
(2012). Chitosan/bioactive glass nanoparticle composite membranes for periodontal
regeneration. Acta Biomaterialia, 8(11), 4173-4180. https://doi.org/10.1016/J.
ACTBIO.2012.06.040
Munarin, F., Guerreiro, S. G., Grellier, M. A., Tanzi, M. C., Barbosa, M. A., Petrini, P., &
Granja, P. L. (2011). Pectin-based injectable biomaterials for bone tissue
engineering. Biomacromolecules, 12(3), 568-577. https://doi.org/10.1021/
BM101110X
Neufeld, L., & Bianco-Peled, H. (2017). Pectin-chitosan physical hydrogels as potential
drug delivery vehicles. International Journal of Biological Macromolecules, 101,
852-861. https://doi.org/10.1016/J.IJBIOMAC.2017.03.167
Neves, S. C., Gomes, D. B., Sousa, A., Bidarra, S. J., Petrini, P., Moroni, L., . Granja, P. L.
(2015). Biofunctionalized pectin hydrogels as 3D cellular microenvironments.
Journal of Materials Chemistry B, 3(10), 2096-2108. https://doi.org/10.1039/
C4TB00885E
Olaru, A. M., Marin, L., Morariu, S., Pricope, G., Pinteala, M., & Tartau-Mititelu, L.
(2018). Biocompatible chitosan based hydrogels for potential application in local
tumour therapy. Carbohydrate Polymers, 179, 59-70. https://doi.org/10.1016/J.
CARBPOL.2017.09.066
Pornpimon, M., & Sakamon, D. (2010). Effects of drying methods and conditions on
release characteristics of edible chitosan films enriched with Indian gooseberry
extract. Food Chemistry, 118(3), 594-601. https://doi.org/10.1016/J.
FOODCHEM.2009.05.027
Sitarz, M., Bulat, K., Wajda, A., & Szumera, M. (2013). Direct crystallization of silicate-
phosphate glasses of NaCaPO 4-SiO2 system. Journal of Thermal Analysis and
Calorimetry, 113(3), 1363-1368. https://doi.org/10.1007/S10973-013-3240-Y/
FIGURES/7
Stroescu, M., Stoica-Guzun, A., Isopencu, G., Jinga, S. I., Parvulescu, O., Dobre, T., &
Vasilescu, M. (2015). Chitosan-vanillin composites with antimicrobial properties.
Food Hydrocolloids, 48, 62-71. https://doi.org/10.1016/J.FOODHYD.2015.02.008
Swamy, M. K., Sinniah, U. R., & Ghasemzadeh, A. (2018). Anticancer potential of
rosmarinic acid and its improved production through biotechnological interventions
and functional genomics. Applied Microbiology and Biotechnology 2018 102:18, 102
(18), 7775-7793. https://doi.org/10.1007/S00253-018-9223-Y
Wajda, A., Bułat, K., & Sitarz, M. (2016). Structure and microstructure of the glasses from
NaCaPO4-SiO2 and NaCaPO4-SiO2-AlPO4 systems. Journal of Molecular Structure,
1126, 47-62. https://doi.org/10.1016/J.MOLSTRUC.2015.12.003
Wajda, A., Goldmann, W. H., Detsch, R., Grünewald, A., Boccaccini, A. R., & Sitarz, M.
(2018). Structural characterization and evaluation of antibacterial and angiogenic
potential of gallium-containing melt-derived and gel-derived glasses from CaO-SiO2
system. Ceramics International, 44(18), 22698-22709. https://doi.org/10.1016/J.
CERAMINT.2018.09.051
Xavier, C. P. R., Lima, C. F., Fernandes-Ferreira, M., & Pereira-Wilson, C. (2009). Salvia
Fruticosa, Salvia Officinalis, and Rosmarinic Acid Induce Apoptosis and Inhibit
Proliferation of Human Colorectal Cell Lines: The Role in MAPK/ERK Pathway.
Http://Dx.Doi.Org/10.1080/01635580802710733, 61(4), 564-571. https://doi.
org/10.1080/01635580802710733.
Xu, C., Zhan, W., Tang, X., Mo, F., Fu, L., & Lin, B. (2018). Self-healing chitosan/vanillin
hydrogels based on Schiff-base bond/hydrogen bond hybrid linkages. Polymer
Testing, 66, 155-163. https://doi.org/10.1016/J.POLYMERTESTING.2018.01.016
Yuliarti, O., Hoon, A. L. S., & Chong, S. Y. (2017). Influence of pH, pectin and ca
concentration on gelation properties of low-methoxyl pectin extracted from Cyclea
barbata Miers. Food Structure, 11, 16-23. https://doi.org/10.1016/J.
FOOSTR.2016.10.005
Zagrajczuk, B., Dziadek, M., Olejniczak, Z., Cholewa-Kowalska, K., & Laczka, M. (2017).
Structural and chemical investigation of the gel-derived bioactive materials from the
SiO2-CaO and SiO2-CaO-P2O5 systems. Ceramics International, 43(15),
12742-12754. https://doi.org/10.1016/J.CERAMINT.2017.06.160
Zhang, Y., Shi, X., Yu, Y., Zhao, S., Song, H., Chen, A., & Shang, Z. (2014). Preparation
and Characterization of Vanillin Cross-Linked Chitosan Microspheres of
Pterostilbene. Http://Dx.Doi.Org/10.1080/1023666X.2014.864488, 19(1), 83-93.
https://doi.org/10.1080/1023666X.2014.864488.
Zhang, M., Yang, M., Woo, M. W., Li, Y., Han, W., & Dang, X. (2021). High-mechanical
strength carboxymethyl chitosan-based hydrogel film for antibacterial wound
dressing. Carbohydrate Polymers, 256, 117590. https://doi.org/10.1016/J.
CARBPOL.2020.117590
Zhou, R., Si, S., & Zhang, Q. (2012). Water-dispersible hydroxyapatite nanoparticles
synthesized in aqueous solution containing grape seed extract. Applied Surface
Science, 258(8), 3578-3583. https://doi.org/10.1016/J.APSUSC.2011.11.119
12