Contents lists available at ScienceDirect
Carbohydrate Polymers
journal homepage: www.elsevier.com/locate/carbpol
# Chitosan characteristics in electrolyte solutions: Combined molecular dynamics modeling and slender body hydrodynamics
Dawid Lupaa, Wojciech Płazinskib,c, Aneta Michna b’*, Monika Wasilewska b,
Paweł Pomastowski d, Adrian Gołębiowski d,e, Bogusław Buszewskid,e, Zbigniew Adamczykb
a M. Smoluchowski Institute of Physics, Jagiellonian University, Łojasiewicza 11, 30-348 Krakow, Poland
b Jerzy Haber Institute of Catalysis and Surface Chemistry, Polish Academy of Sciences, Niezapominajek 8, PL-30239 Krakow, Poland
c Department of Biopharmacy, Medical University of Lublin, ul. Chodźki 4A, 20-093 Lublin, Poland
d Centre for Modern Interdisciplinary Technologies, Nicolaus Copernicus University, Wilenska 4, 87-100 Torun, Poland
e Department of Environmental Chemistry and Bioanalytics, Faculty of Chemistry, Nicolaus Copernicus University, Gagarin 7, 87-100 Torun, Poland
H)
Check for
updates
ARTICLE INFO
ABSTRACT
Keywords:
Chitosan molecule conformations Chitosan molecule charge Hydrodynamic diameter Molecular dynamics modeling Intrinsic viscosity
Zeta potential
Molecular dynamics modeling was applied to predict chitosan molecule conformations, the contour length, the gyration radius, the effective cross-section and the density in electrolyte solutions. Using various experimental techniques the diffusion coefficient, the hydrodynamic diameter and the electrophoretic mobility of molecules were determined. This allowed to calculate the zeta potential, the electrokinetic charge and the effective ioni­zation degree of the chitosan molecule as a function of pH and the temperature. The chitosan solution density and zero shear dynamic viscosity were also measured, which enabled to determine the intrinsic viscosity increment. The experimental results were quantitatively interpreted in terms of the slender body hydrodynamics exploiting molecule characteristics derived from the modeling. It is also confirmed that this approach can be successfully used for a proper interpretation of previous literature data obtained under various physicochemical conditions.

* Corresponding author.
E-mail addresses: dawid.lupa@uj.edu.pl (D. Lupa), wojtek_plazinski@o2.pl (W. Plazinski), aneta.michna@ikifp.edu.pl (A. Michna), monika.wasilewska@ikifp. edu.pl (M. Wasilewska), pomastowski.pawel@gmail.com (P. Pomastowski), adrian.golebiowski@doktorant.umk.pl (A. Gołębiowski), bbusz@umk.pl (B. Buszewski), zbigniew.adamczyk@ikifp.edu.pl (Z. Adamczyk).
https://doi.org/10.1016/j.carbpol.2022.119676
Received 19 March 2022; Received in revised form 11 May 2022; Accepted 27 May 2022
Available online 30 May 2022
0144-8617/© 2022 The Authors. Published by Elsevier Ltd. This is an open access article under the CC BY license (http://creativecommons.org/licenses/by/4.0/).
## 1. Introduction
Chitosan is a linear polysaccharide derived from naturally occurring chitin - the second most abundant biopolymer (Kaczmarek et al., 2019) - by its partial deacetylation in enzymatic or base-catalyzed processes. A backbone of chitosan molecule is composed of randomly distributed D- glucosamine (2-amino-2-deoxy-₽-D-glucopyranose, deacetylated unit, GlcNH2) and W-acetyl-D-glucosamine (2-acetamido-2-deoxy-₽-D-gluco- pyranose, acetylated unit, GlcNAc) linked with p-(1	4) bonds, as
shown in Fig. 1. Depending on the chitin source and deacetylation process conditions, the molar mass of chitosan varies from 65 to 25,000 kDa (Errington et al., 1993; Morris et al., 2009; Wang et al., 1991).
Among chitosan applications, especially in the biomedical and food context, a tendency to form hydrogel seems to be the most important. Chitosan hydrogels are effective in the targeted adsorption of dyes and proteins from aqueous solutions as was reported by Boardman et al. (2017). Furthermore, chitosan itself has also a high impact on the gelatinization, gel formation, and retrogradation of maize starch as was proved by Raguzzoni et al. (2016).
Because of its biocompatibility, biodegradability and low toxicity, chitosan-based materials have been thoroughly investigated as a component of chitosan-casein hydrophobic peptides nanoparticles, used as soft Pickering emulsifiers (Meng et al., 2022), for application as antimicrobial agents (Chien et al., 2016), in 3D printing of biocompat­ible scaffolds (Rajabi et al., 2021; Suo et al., 2021) in wound healing (Bano et al., 2019); (Patrulea et al., 2015), in cosmetics and food products as stabilizers (Saha & Bhattacharya, 2010), (Harding et al., 2017), rheology modifier (thickener), in household and commercial products (Pini et al., 2020; Wardy et al., 2014), for producing macroion films in the layer-by-layer processes at various substrates, comprising targeted drug delivery systems based on nanoparticle cores. Chitosan and its derivatives have also gained much attention due to their unusual properties allowing for adsorption and then effective removal of different types of dyes and heavy metal ions (Wan Ngah et al., 2011;
Vakili et al., 2014).
The properties of chitosan solutions were widely studied with the aim to evaluate its molar mass distribution (Hasegawa et al., 1994); the radius of gyration and contour length (Colfen et al., 2001); (Weinhold & Thoming, 2011), persistence lengths (Berth & Dautzenberg, 2002; Morris et al., 2009), the hydrodynamic diameters and the second virial coefficients (Anthonsen et al., 1993; Berth & Dautzenberg, 2002; Errington et al., 1993). Furthermore, it was found that the physico­chemical properties of solutions can be modified by controlled chitosan dispersion in various organic acids (Soares et al., 2019).
A plethora of works was devoted to investigations of rheological properties of chitosan solutions, especially the intrinsic viscosity [n] under various physicochemical conditions. An analysis of the available experimental data is presented in Fig. S1 in Supporting Information. Many attempts were undertaken in the literature to rationalize these results characterized by a considerable scatter in terms of the empirical Mark-Houwink (MH) relationship connecting the intrinsic viscosity [n] with the molar mass, Mp
[n] = KMp	(1)
where Mp is expressed in Da, K (usually expressed in dL g ~1) and a (dimensionless) are empirical constants depending on various parame­ters, primarily on ionic strength and electrolyte composition, pH, the acetylation degree, the temperature, the molar mass range, the stability of the chitosan solutions, aggregation degree etc. A significant scatter of the fitting parameters was reported in the literature, with K varying between 3 x 10 7 to 1.115 x 10 2 dL g ~1 and a ranging between 0.147 and 1.26 (Kasaai, 2007) or even 1.37 for ionic strength of 0.005 M (Anthonsen et al., 1993). This hinders a proper theoretical interpretation of experimental data and limits the precision of the MH equation often used for a facile molar mass determination, especially of commercial chitosan samples. The parameters of the MH equation reported for different parameters are collected in Fig. S2.
It should also be mentioned that the experimental intrinsic viscosity having the dimension of dL g 1 depends on the density of macroion molecules pp. This prohibits its proper physical interpretation in terms of hydrodynamic models, which postulate that the viscosity of dispersion is independent of the particulate matter density. As discussed in recent works (Adamczyk et al., 2018); (Michna et al., 2021), instead of [n], the intrinsic viscosity increment uexp = pp[n] (Morris et al., 2009) is the parameter prone to a sound physical interpretation. However, the calculation of uexp requires the macroion molecule density to be simul­taneously determined with the viscosity measurements. Unfortunately, such a procedure was not used in the literature except for the work of Errington et al. (1993).
Therefore, to increase understanding of chitosan molecule behav­iour, a more quantitative approach was applied in this work, founded on the combination of molecular dynamics (MD) modeling with low Rey­nolds number hydrodynamics. Performed calculations furnished various parameters prone to experimental measurements such as the molecule diffusion coefficient, gyration radius and the intrinsic viscosity incre­ment. The obtained theoretical results were used for the interpretation of experimental data acquired using various techniques such as Fourier transform infrared spectroscopy (FTIR), the dynamic light scattering (DLS), micro-electrophoresis (LDV), matrix-assisted laser desorption/ ionization coupled to time of flight mass spectrometry (MALDI-TOF/ TOF MS), asymmetric flow field-flow fractionation coupled with multi­angle light scattering (AF4-RI-MALS), the optical waveguide lightmode spectroscopy (OWLS) and the zero shear rate dynamic viscosity mea­surements. As a result, a quantitative information about the physico­chemical properties of chitosan molecule such as the chain conformations and length, effective ionization degree and the number of uncompensated charges as a function of pH and the temperature was acquired.
## 2. Materials and methods
### 2.1. Materials
Chitosan sample (lot no. 448869) was supplied by Sigma-Aldrich (Poland) in the form of powder. The molar mass (determined by the viscosity method) given by the producer lies in the range of 50 to 190 kg mol 1 (kDa) with an average value of 120 kg mol 1. Detailed charac­terization of obtained chitosan sample is given in Supporting Information.
NaOH and HCl were analytical grade products of Avantor Perfor­mance Materials Poland S.A. All reagents were used as received. Pure water of resistivity 18.2 MQ was obtained using Milli-Q Elix & Simplicity 185 purification system from Millipore SAS Molsheim, France.
### 2.2. Methods
The solutions of chitosan were prepared by dissolving a proper amount of the powder in 0.01 M HCl. When necessary, the pH of solution was increased using a proper volume of 1 M NaOH by keeping ionic strength at a constant level.
Elemental composition of the chitosan sample, especially the C/N atomic ratio was determined using Thermo Scientific FlashSmart Elemental Analyzer. Additionally, the presence of characteristic moi- eties and DA value were evaluated using FTIR (FTIR Nicolet 6700 spectrometer, Thermo Scientific). FTIR spectrum was acquired using the classical KBr pellet method.
The molar mass of chitosan was acquired by AF4-RI-MALS and MALDI-TOF/TOF MS analysis.
The distribution of molar mass and radius of gyration was also determined using Postnova AF2000 MultiFlow system (Postnova Ana­lytics GmbH, Landsberg am Lech, Germany). 10 kDa membrane made out of regenerated cellulose and 350 ^m spacer were used in this study.
A RI detector PN3150 (Postnova Analytics GmbH, Landsberg am Lech, Germany) was applied for determining particle concentration.
MALS detector PN3621 (Postnova Analytics GmbH, Landsberg am Lech, Germany) collected data at angles from 12° to 164°; the temper­ature of the detector cell was set to 35 °C with 80% laser (2 = 532 nm) power. As a carrier liquid, the 0.01 M HCl solution was used (Merck KGaA, Darmstadt, Germany) filtered through a 0.1 ^m nylon membrane (Merck Millipore, Warsaw, Poland). The injection volume was 100 ^L.
Fig. 1. A schematic representation of the chemical structure of the chitosan molecule with the functionalization motif used in the MD simulations. The acetylation degree (DA) is 40%. The IUPAC-recommended numbering of some atoms and definition of glycosidic dihedral angles are given as well.

All fractionation analyses were performed at room temperature.
The fractionation method was adopted from (Gonzalez-Espinosa et al., 2019) with some modifications. The detector flow was 0.5 mL min 1. The injection and focusing steps of fractionation consist of 0.2 mL min 1 injection, 3.3 mL min 1 focusing and 3.0 mL min 1 cross­flows through 6 min and then 0.2 min of transition to the elution step. The elution is based on an exponential (0.4) decrease in cross flow to 0.06 mL min -Lvalue. The constant flows were kept to elute all fractions. Evaluation of the data was performed using AF2000 Control software using the Zimm function. Chitosan sample was prepared with a con­centration of2000 mg L 1 in 0.01 M HCl, which was dissolved by mixing for at least 2 h. According to (Czechowska-Biskup et al., 2007) dn/dc value for chitosan in HCl solution is 0.146 mL g 1.
A MALDI-TOF/TOF MS instrument equipped with a modified neodymium-doped yttrium aluminium garnet (Nd: YAG) laser (1-kHz Smartbeam-II, Bruker Daltonik) operating at the wavelength of 355 nm was used for all measurements. All spectra were acquired in linear positive mode using an acceleration voltage of 25 kV within a m/z range of 30,000 to 500,000 at 50% of laser power and a global attenuator of 30%. All mass spectra were acquired and processed using dedicated software, flexControl and flexAnalysis, respectively (both from Bruker Daltonik).
For MALDI-TOF/TOF MS analysis, chitosan solution was prepared in 0.01 M HCl and 0.1% TFA in water. The analysis was performed using three different matrices - HCCA, DHB and SA. Equal amounts of satu­rated HCCA solution in TA30 and sample were applied to the plate and allowed to dry. The same protocol was used for DHB (20 mg ml 1 in TA30). In contrast, a double layer protocol was used for SA. A saturated solution of SA in EtOH was applied to the plate and allowed to dry. The sample solution and saturated SA in TA30 were then applied to the first layer.
The high-resolution mass spectra of chitosan determined by MALDI- TOF/TOF MS as well as a molar mass distribution, and radius of gyration determined by AF4-RI-MALS were presented in Figs. S6-S8 and Table S3.
The diffusion coefficient and the electrophoretic mobility of chitosan molecules for various pHs were determined using DLS and LDV, respectively. Both DLS and LDV experiments were performed using Malvern Zetasizer Nano ZS apparatus. Chitosan concentration was kept at 100 and 300 mg L 1 in the case of the diffusion coefficient and the electrophoretic mobility determination, respectively. The Ohshima (2012) and Einstein (1908) equations were applied to calculate the zeta potentials and the hydrodynamic diameters of chitosan using the elec­trophoretic mobility and the diffusion coefficient data.
Additionally, the hydrodynamic diameter of chitosan molecules was determined at a low concentration range (typically 5 mg L 1 inacces­sible to DLS) using the method based on adsorption kinetics measure­ments in a microfluidic flow cell (for details consult Fig. S12). Accordingly, the chitosan molecule adsorption was measured using the optical wave-guide spectroscopy (OWLS) according to the procedure previously described in Refs. Wasilewska et al. (2019) and Michna et al. (2020). The OWLS 210 instrument (Microvacuum Ltd., Budapest, Hungary) was used. The apparatus is equipped with a laminar slit shear flow cell comprising a silica-coated waveguide (OW2400, Micro­vacuum). The adsorbing substrates were planar optical waveguides made of a glass substrate (refractive index 1.526) covered by a film of Si0.78Ti0.22O2 (thickness 170 nm, refractive index 1.8). A grating embossed in the substrate enables the light to be coupled into the waveguide layer. The sensor surface was coated with an additional layer (10 nm) of pure SiO2 according to the previous protocol (Wasilewska et al., 2019). The adsorption kinetic measurements yielded the mass transfer rate of chitosan molecules, which was converted to the diffusion coefficient and in consequence to the hydrodynamic diameter using the Stokes-Einstein relationship (Eqs. S9-S13 in Supporting Information).
The density of chitosan solutions of defined mass fraction (wp) was determined using the Anton Paar DMA 5000 M densitometer. This apparatus was coupled with the Anton Paar rolling-ball viscometer Lovis 2000 M/ME equipped with a short capillary tube, which allowed simultaneous determination of the dynamic viscosity of solutions with a large precision (0.05%) using relatively small volumes of chitosan so­lutions (0.1 mL). The zero-shear dynamic viscosity was calculated by extrapolation of dynamic viscosity determined at different shear rates (capillary tilt angles). A description of measurement principles can be found elsewhere (Michna et al., 2021). The measurements were carried out for chitosan mass fractions below 10 3 (dilute macroion concen­tration limit) and at a fixed ionic strength 0.01 M.
All experiments were performed in triplicates.
### 2.3. Molecular dynamics modeling
A series of chitosan chains of various lengths, composed of 5, 10, 20 and 40 monosaccharide residues (referred to later on as monomers) was considered in the molecular dynamics simulations. The acetylation de­gree DA of 40% was reflected by the composition of the chains, which contain the periodically repeating motif of functionalization: -GlcNH3+- GlcNH3+-GlcNAc-GlcNH3+-GlcNAc-, see Fig. 1.
The initial configurations of the systems, including the chain solva­tion as well as the addition of co-ions were created using the CHARMM- GUI online server (Park et al., 2019). The systems of interest consisted of cubic boxes of the initial edge dimensions varying from 4.9 to 21.6 nm, depending on the system. The number of water molecules included in simulation boxes varied from 3800 to 322,500, respectively. The appropriate number of Na+ and Cl ions was added to each system, accounting for its neutral charge and the desired ionic strength value (0.01 M).
The all-atom molecular dynamics (MD) modeling were carried out within the GROMACS 2016.4 package (Abraham et al., 2015). The CHARMM36 force field (Guvench et al., 2011) was used to describe the interactions involving chitosan molecules, accompanied by the CHARMM-compatible explicit TIP3P water model (Jorgensen et al., 1998). According to the assumed pH conditions, all amine groups in the chitosan chain were assumed to be protonated and bear a formal posi­tive charge. The parameters describing the protonated amine moieties were prepared manually and relied on the parameters generated by the ligand builder module of the CHARMM-GUI server.
The modeling was carried out applying periodic boundary conditions and in the isothermal-isobaric ensemble. The temperature was main­tained close to its reference value (298 K) by applying the V-rescale thermostat (Bussi et al., 2007), whereas for the constant pressure (1 bar, isotropic coordinate scaling) the Parrinello-Rahman barostat (Parrinello & Rahman, 1981) was used with a relaxation time of 0.4 ps. The equations of motion were integrated with a time step of 2 fs using the leap-frog scheme (Hockney, 1970). The hydrogen-containing solute bond lengths were constrained by the application of the LINCS proced­ure with a relative geometric tolerance of 10 4 (Hess, 2008). The full rigidity of the water molecules was enforced by the application of the SETTLE procedure (Miyamoto & Kollman, 1992). The electrostatic in­teractions were modeled by using the particle-mesh Ewald method (Darden et al., 1998) with a cut-off set to 1.2nm, while van der Waals interactions (LJ potentials) were switched off between 1.0 and 1.2 nm. The translational center-of-mass motion was removed every timestep separately for the solute and the solvent.
The systems were subjected to geometry minimization and MD-based equilibrations in the NPT ensemble, lasting 5-20 ns, depending on the system size. After equilibration, production simulations were carried out for a duration of 100-130 ns and the data were saved to trajectory every 2 ps. The end-to-end, persistence length and gyration radius values were calculated by using the GROMACS routines gmx polystat and gmx mindist. The anomeric carbon atoms were selected to define the polymer back­bone in the case of the longest chain and calculations aimed at persis­tence length.
The final frames of the equilibration trajectory of the system
containing decameric chains of chitosan were used to initiate enhanced- sampling free energy calculations carried out according to the protocol described below. The calculation of the 2D free energy maps (FEMs) relied on an enhanced-sampling scheme combining parallel tempering (Earl & Deem, 2005) and well-tempered metadynamics (Barducci et al., 2008) as implemented in the PLUMED 2.3 plug-in (Tribello et al., 2014). The well-tempered metadynamics simulations involved a 2D space of collective variables defined by the values of the and y glycosidic dihedral angles. They were defined by the following quadruplets of atoms:	= O5-C1-O1-C'4, y = C1-O1-C'4-0'3. The parameters of meta­
dynamics were set as follows: initial height of bias portion: 0.1 kJ/mol, bias portion width: 0.314 rad, deposition rate: 0.5 kJ/mol/ps, bias factor (dependent on the AT parameter in Eq. (2), ref. (Barducci et al., 2008)): 10. The parallel-tempering relied on 16 metadynamics simulations carried out in parallel at different temperatures ranging from 298.0 to 363.2 K in steps of about 4.3 K, along with replica-exchange attempts performed at 2 ps intervals. All metadynamics simulations were carried out for 10 ns.
## 3. Results and discussion
### 3.1. Theoretical modeling results
As mentioned, the calculations were performed for chitosan chains composed of 5, 10, 20 and 40 monomers characterized by the average molar mass 0.179 kg mol 1. The results of this MD modeling enabled to determine the molecule conformation, the time-averaged gyration radius, the end-to-end distance and the extended (contour) length as a function of the degree of polymerization, denoted by DP. The derivative parameters such as the persistence length, the extended chain diameter and the molecule density were also theoretically predicted.
Exemplary snapshots of chitosan chain conformations obtained for NaCl concentration of 0.01 M and different polymerization degree are shown in Fig. 2. Qualitatively, one can observe that the chains contain quasi-rigid fragments, but also some kinks, corresponding to reoriented glycosidic linkages. This type of conformation can be traced back to the flexibility of the individual glycosidic linkages between mono­saccharides composing the chain, as studied by the additional, meta­dynamics simulations.
The resulting free energy maps (FEMs, Fig. 3) calculated with respect to the glycosidic dihedral angle values show that the general landscape is roughly independent of the monosaccharide functionalization, i.e. the
Fig. 2. Snapshots of chitosan chain conformations for systems composed of 10, 20 and 40 residues, derived from MD modeling. Solvent molecules are omitted for clarity, 0.01 M NaCl.
location of either the global or local minima on FEM remains unaltered by the substitution of the neighbouring residues. Moreover, the FEM area corresponding to the low (< 5 kJ/mol) free energy levels covers only a narrow fraction of the map, which indicates preferences for a relatively rigid conformation of a given linkage. However, the energy level corresponding to the secondary free energy minima on FEM calculated for the GlcNH3+- GlcNAc linkage is located close to the zero­level of energy which indicates enhanced flexibility of such linkage, compared to the remaining ones (levels of ca. -7.5 kJ/mol vs. ca. -12 kJ/ mol). This corresponds to the population of the alternative chain ge­ometries ca. 5%. Apart from that, an additional, tertiary minimum at the relatively low level of ca. -9 kJ/mol can be observed. Considering the large abundance of this type of linkages and the possible contribution of the remaining linkage types, one has to assume the non-negligible in­fluence of the non-standard conformers of the residue-residue linkage on the overall chain geometry.
Fig. 3. The free energy maps calculated by metadynamics modeling and illustrating the inherent flexibility of glycosidic linkages between various monosaccharide residues within the chitosan chain: (A) GlcNH+-GlcNAc linkage; (B) GlcNAc-GlcNH+ linkage; (C) GlcNAc-GlcNAc linkage. $ and 1/ denote glycosidic dihedral angles, defined according to the IUPAC notation. Energy scale is in [kJ/mol].
The intramolecular hydrogen bonding included mainly interactions between the O5 ring oxygen atoms and -OH groups of the two consec­utive monosaccharide residues. However, the quantitative occurrences of intramolecular hydrogen bonding per 1 residue are low (0.52 per timeframe), indicating the limited intensity of such interaction types and preferred interactions with water molecules instead (6.48 solute-solvent hydrogen bonds per 1 residue). Apart from the conformationally- restricted mutual orientation of the neighbouring residues, no ten­dency to the formation of regular, helical shapes within a larger dimensional scale was observed.
The MD modeling also allowed to quantitatively determine the time- averaged gyration radius Rg and the average end-to-end distance of the molecule Lete (for 0.01 M HCl) as a function of DP. These dependencies are illustrated in Fig. 4. One can observe that these parameters can be well fitted by following linear dependencies
Rg = 0.227 + 0.119DP	(2)
where: Rg is expressed in [nm]
Lete = 0.681 + 0.336DP	(3)
where: Lete is expressed in [nm].
Assuming that DP is equal to zero, Eqs. (2) and (3) will provide non­physical results. As the data used to obtain the best-fit parameters were generated for chains of a minimal length of 5 residues, the extrapolation below this value, where end-effects may play a more substantial role, is associated with larger errors of predictions, leading ultimately to non­zero Rg and Lete for DP = 0. In spite of that, the relative magnitude of such errors is rather small when referring to the absolute values of both quantities determined for longer chains.
On the other hand, the maximum end-to-end distance, which can be interpreted as the contour length of the fully extended molecule was interpolated by the dependence.
Lete max = 0.083 + 0.454DP
where: Lete max is expressed in [nm].
(4)
The latter dependence allowed to determine the residue contour length, which was 0.460 nm (see Table 1). Additionally, the persistence length determined during MD simulations and based on the ‘backbone' defined by anomeric carbon atoms is 5.0 nm. For comparison, the experimental values reported in the literature vary between 4.5 (Schatz et al., 2003) and 7.6 nm (Lamarque et al., 2005).
The density of the chitosan molecule was calculated using the pre­viously applied method (Adamczyk et al., 2018). Accordingly, the size of the simulation boxes, where a single chitosan molecule was confined, was systematically increased, resulting in the decrease in the chitosan mass fraction from 0.02 to 0. The density of these systems ps, as well as that of the pure solvent pe, were determined in additional MD runs. Then, the dependence of pe/ps on wp was plotted and fitted by a straight line characterized by the slope sp and the density was calculated from the formula:
Pe
Pp
Dependences of the relative densities of the chitosan solutions on the mass fraction determined by two complementary approaches: molecular dynamics (MD) modeling and densitometry were presented in Fig. S4, Fig. S5 and Table S2, respectively.
(5)
1 + sp
It was determined that, at the temperature of 298 K (0.01 M HCl), the density of the bare chitosan chain (no hydration) was 1.82 x 103 kg m 3. This value can be rescaled upon assumption that each residue in a chain is accompanied by either water molecule(s) (chain hydration) or coun­terions (ion condensation occurring in the case of charged residues). For instance, the density for the hydrated chain is 1.49 x 103 kg m 3 (Table 1). For comparison, the experimental value reported by Errington et al. (Errington et al., 1993) for DA = 58% in 0.2 M NaCl was 1.72 x 103 kg m 3. It should be mentioned that molecule density is the indis­pensable parameter for a proper hydrodynamic interpretation of the experimentally derived intrinsic viscosity.
Using the densities of 1.82 x 103 kg m 3 and 1.49 x 103 kg m 3 one can calculate the average volume of a monomer from the dependence V1 = M1/(PpNA) which was 0.163 and 0.200 nm3 for the cases of bare chitosan chain and hydration accompanying one water molecule per residue, respectively (Table 1). Consequently, assuming its cylindrical shape and considering that its molar mass is 0.179 kg mol \ the equivalent monomer diameter calculated as d1 = (4v1/nlm)1/2 was 0.672 and 0.744 nm, respectively.
Similar values of the extended chain diameter 0.662 and 0.733 nm, for no hydration and hydration with one H2O molecule per monomer, respectively, were obtained from direct MD modeling. For this purpose,

Fig. 4. (A) The average gyration radius (Rg) calculated from the results of MD modeling vs. the degree of polymerization (DP) (B) The average end-to-end length (Lete) vs. DP (C) The maximal values of the end-to-end length (Lete max) vs. DP. The solid line denotes the linear fitting of theoretical data. Vertical bars in panels (A) and (B) denote the fluctuations of the given quantity found during MD modeling and expressed as standard deviation values.

the density-dependent monomer volume was multiplied by the numbers of mers in the individual chain and related to the monomer length determined for the shortest chain. These data correspond to a negligible ionic strength limit.
On the other hand, for the ionic strength of 0.01 M, the chain diameter was 0.731 and 0.809 nm, for no hydration and hydration, respectively.
The theoretically-determined extended monomer contour length (0.460 nm) agrees reasonably well with the experimental values of 0.49 (Lamarque et al., 2005) and 0.515 nm (Korchagina & Philippova, 2010).
Table 1
Primary physicochemical characteristics of the chitosan molecule derived from MD modeling, 0.01 M HCl, 40% periodic acetylation (DA).
Quantity [unit], symbol	Value	Remarks
Monomer molar mass	0.179	Average value for protonated amine
[kg mol_ 1], Mi		groups
Extended monomer	0.460 ±	This work, MD modeling, fully extended
contour length [nm],	0.02	chain
lm	0.515	DA = 0.05, (Korchagina & Philippova, 2010)
	0.49	DA = 0.40, (Lamarque et al., 2005)
Persistence length [nm],	5.0	This work, MD modeling
Lp	7.6	DA = 0.40 (Lamarque et al., 2005)
	4.5	(Schatz et al., 2003)
	5	(Rinaudo et al., 1993)
Molecule density [kg	1.82 ±	This work, MD modeling, no hydration
m 3], Pp	0.10 X 103
	1.49 ±	This work, MD modeling, hydration of 1
	0.10 X 103	water molecule / per protonated monomer
	1.35 ±	This work, MD modeling, with
	0.10 X 103	condensation of one Cl_ ion per one protonated monomer
	1.72 X 103	DA = 0.58, Errington et al. (1993)
Monomer volume [nm3],	0.163	This work, no hydration, calculated as Vi
Vi		= Mi/(ppAv)
	0.200	This work, hydration
	0.221	Ion condensation
Monomer equivalent	0.672 ±	This work, no hydration, calculated as dc
cylinder diameter	0.03	= (4Vi/nlm)
[nm], dc	0.744 ± / 0.03	This work, hydration
	0.781 ± / 0.03	This work, ion condensation
Extended chain diameter	0.662 ±	No hydration, calculated from contour
[nm], dex	0.03	length
	0.733 ± / 0.03	This work, hydration
	0.769 ± / 0.03	Ion condensation
Chain diameter [nm]	0.731 ±	No hydration, calculated from the
	0.03	average end-to-end Distance value / for 0.01 M HCl
	0.809 ± / 0.03	Hydration, 0.01 M HCl
	0.849 ± / 0.03	Ion condensation, 0.01 M HCl

The agreement is even better when using the corresponding value relying only on the MD simulations of the shortest chain (0.474 nm) which is the most extensively sampled, providing probably the most accurate maximal extended chain value. Minor differences between theoretical predictions and the experimental data are expected due to the following factors: (i) deviations in the system composition with respect to the real systems (this includes both the necessary restrictions in the system size and the uncertain pattern of acetylation which does not necessarily correspond to the periodic one assumed in our MD simulations); (ii) sampling-inherent inaccuracies. The latter issue con­cerns mainly the persistence length as it cannot be determined using the enhanced-sampling metadynamics technique and is possible to be esti­mated only for sufficiently long chains (it was possible only for the longest chain in the case of presently studied systems) and, at the same time, is slowly converging variable. The presently estimated value of 5.0 nm is close to the lower limit of experimentally-inferred values, to the MD-relying value of 5 nm by Singhal et al. (Singhal et al., 2020) and persistence lengths calculated by Tsereteli and Grafmüller using the coarse-grained model and varying in the range of 6-9 nm (Tsereteli & Grafmüller, 2017). The latter work is also in line with our finding stating that the GlcNH3+-GlcNAc linkage is the most flexible one.
One should expect that the extrapolation of these results to a larger molar mass of chitosan furnishes useful data inaccessible for direct theoretical modeling because of excessive time of computations.

However, it is to remember that this only concerns chitosan samples of low dispersity.
### 3.2. Experimental characteristics of chitosan
Dry mass of chitosan powder was determined using classic ther­mogravimetry. The detailed protocol for these measurements can be found in Section 2.1 in Supporting Information. Such experiments showed that the water content in the chitosan sample was 8%.
Elemental composition of the chitosan sample, especially the C/N atomic ratio was determined using elemental analysis. Additionally, the presence of characteristic moieties and DA value were evaluated using Fourier transform infrared spectroscopy (FTIR).
It was 37% ± 3 and 39% ± 2, respectively. It was assumed that the distribution of the -NH2 groups was quasi-periodic, as in theoretical modeling (see Fig. 1).
The calculation of DA, a spectrum of the chitosan sample and the most significant peaks visible in the spectrum, as well as their assign­ment to respective vibrations, were collected in Fig. S3 and Table S1, respectively.
The chitosan molecule density for various temperatures was deter­mined by the dilution method according to the procedure described previously (Adamczyk et al., 2018). The primary results shown in Fig. S5 enabled to calculate the density from Eq. (5) using the slope of pe/ps vs. the mass fraction of chitosan in the solution, wp analogously as for the theoretical modeling. In this way, one obtained 1.5 ± 0.2 x 103 and 1.55 ± 0.02 x 103 kg m 3 for the temperature of 298 K and 308 K, respec­tively. It is noteworthy here that the value of ps determined at 298 K agrees with the result derived from MD modeling.
On the other hand, the molar mass of the chitosan sample deter­mined by AF4-RI-MALS and MALDI-TOF/TOF MS was 412 and 346 kg mol 1 (kDa), respectively. These values differ significantly from the molar mass given by the producer, 50 to 190 kg mol ~1 (average value 120 kg mol 1), as determined by a viscosity method. However, such discrepancy is common for chitosan samples, where the molar mass derived for osmotic pressure measurements and MALS may differ in some cases by a factor up to 4.6 (Anthonsen et al., 1993). This is mainly attributed to the sample aggregation during the measurements. As shown in Ref. (Korchagina & Philippova, 2010) for the chitosan sample with Mp = 125 kDa, approx. 10% of chitosan chains are forming spherical aggregates characterized by an aggregation number of ca. 10.
Therefore, in this work except for the dynamic viscosity measure­ments, a few complementary methods were applied to derive informa­tion about the chitosan and conformations of its molecule in electrolyte solutions. Primarily, the dynamic light scattering (DLS) measurements were carried out yielding the diffusion coefficient of molecules from the light intensity autocorrelation function. The advantage of DLS method, compared to the static light scattering (MALS) is that no column sepa­ration of the sample is needed and that the signal is independent of the molecule shape. Additionally, macroion samples characterized by sig­nificant dispersity can be analyzed at a relatively low concentration range.
Extensive measurements discussed in Supporting Information enabled to determine the chitosan molecule diffusion coefficient as a function of pH varied between 2 and 6, for a fixed ionic strength of 0.01 M NaCl (see Fig. S9). Also, the dependence of the diffusion coefficient on the storage time was measured for various pHs in order to determine the chitosan solution stability. Finally, the dependence of the diffusion co­efficient on the temperature, which varied between 293 and 323 K, was experimentally determined (see Fig. S10 part A). These data were con­verted to the molecule hydrodynamic diameter dH using the Stokes­Einstein relationship (Einstein, 1908)
where: k is the Boltzmann constant, T is the absolute temperature, n is the dynamic viscosity of the electrolyte and D is the diffusion coefficient of the molecule derived from DLS.
It is revealed that there were two main fractions were present in the chitosan sample: the first one characterized by the hydrodynamic diameter of 19 ± 2 nm (number averaged) and the other exhibiting dH = 40 ± 5 nm (also number averaged). Interestingly, the former value was fairly independent of pH and the storage time up to 72 h, which is illustrated in Fig. 5.
It is also observed that the hydrodynamic diameter at pH 2 (for the primary peak) decreased from 20 to 15 nm upon an increase of the temperature from 293 to 323 K (Fig. S10 part B).
It is interesting to compare the chitosan molecule hydrodynamic diameter derived from DLS with the diameter of an equivalent sphere ds calculated as:
ds =
' 6Mp ) 1/3
KppNA
(7)
For Mp = 50 kDa one obtains from Eq. (7) ds = 4.7 nm. For Mp = 120 kDa (average value given by the producer), one obtains ds = 6.3 nm. These values are significantly smaller than the DLS hydrodynamic diameter. This indicates that at an ionic strength of 0.01 M the chitosan molecule assumes a largely elongated shape, analogously as previously observed for other macroions (Adamczyk et al., 2018); (Michna et al., 2021). Therefore, it is reasonable to theoretically interpret the DLS re­sults using the slender body hydrodynamics pertinent to the case where the length to width ratio (aspect ratio) of a molecule denoted by A considerably exceeds unity (Brenner, 1974). For such a case the hy­drodynamic diameter can be expressed in the following form (Mansfield & Douglas, 2008); (Adamczyk et al., 2012):
dH =
Lc
c 1 ln2A + c2
= dc
A
c1 ln2A + c2
(8)
where Lc is the contour length of the molecule, c1, c2 are the dimen­sionless constants depending on the shape of the body and dc is the molecule chain diameter.
For prolate spheroids one has c1 = 1, c2 = 0; for blunt cylinders: c1 = 1, c2 = — 0.11; (Brenner, 1974) for linear chain of touching beads:c1 = 1, c2 = 0.25 and for a chain of beads forming a torus one has: c1 = 11/12,
Fig. 5. The dependence of the hydrodynamic diameter of the chitosan molecule (first fraction) on pH and the storage time, I = 0.01 M; T = 298 K; bulk solution concentration 100 mg L 1. The dashed line denotes the average value of dH = 19 ± 2 nm.
. = kT H 3nnD
(6)

Rg
L
121/2
(9)
Fig. 6. The dependence of the electrophoretic mobility and the number of elementary charges per one chitosan molecule on pH. Measurement conditions: I = 0.01 M; T = 298 K; bulk solution concentration 300 mg L 1. The solid line denotes the logistic fit of experimental results.
c2 = 0.67 (Adamczyk et al., 2006). Replacing the string of touching beads by a flexible cylinder of the same volume and length one obtains c1 = 1, c2 = — 0.45 (linear chain) and c1 = 11/12, c2 = 0.48 (torus) (Adamczyk et al., 2006).
The Lc parameter appearing in Eq. (8) can be calculated as lmMp/M1 using the monomer contour length lm given in Table 1. For the extended chain (this corresponds to a low ionic strength limit) one has lm = 0.460 nm, whereas for the 0.01 M ionic strength one has lm = 0.378 nm. Using also the chain diameter of 0.733 nm (Table 1) one can calculate that for the molar mass of 50 kDa, where Lc = Lex = 280 nm, the hydrodynamic diameter predicted from Eq.(8) is 21.9, 22.3 and 21.9 nm for spheroid, cylinder and torus, respectively. Analogously, for I = 0.01 M, where Lc = 105 nm and the chain diameter is 0.809 nm one obtains dH = 18.6, 18.9 and 18.6 nm for spheroid, cylinder and torus. As can be seen, these values little depend on the molecule shape and agree within the error bound with the experimental value (DLS) 19 nm.
For the average molar mass of 120 kDa, Lex = 308 nm, and dH = 45.7, 46.5 and 46.3 nm for the spheroid, cylinder and torus, respectively, in the low ionic strength limit. Analogously, for 0.01 M ionic strength one obtains dH = 39.2, 39.8 and 39.5 nm for the spheroid, cylinder and torus. Again, these values agree with the experimental hydrodynamic diameter derived from DLS (40 nm) for the second chitosan fraction. It is also worth mentioning that in Ref. (Korchagina & Philippova, 2010) a similar value of the hydrodynamic diameter 36 ± 4 nm was reported for an unaggregated chitosan sample having the molar mass of 125 kDa and DA = 5%.
Interestingly, for the straight cylinder conformation, the gyration radius becomes independent of the chitosan molecule diameter and can be calculated from the formula (Adamczyk et al., 2021)
Thus, for the molar mass of 50 kDa one can calculate from Eq. (9) that the gyration radius is 37 and 30.3 nm, in the limit of low ionic strength and for 0.01 M, respectively. Analogously, for the molar mass of 120 kDa, the gyration radius is 88.9 and 72.7 nm for these two cases, respectively.
Independently, the hydrodynamic diameter of chitosan molecules was determined as described above using OWLS, which yielded repro­ducible results for the low solution concentration of 5 mg L 1 where the interaction among chitosan molecules become negligible. Primarily, in these experiments, the adsorption kinetics of chitosan expressed as the mass coverage vs. the time dependence was determined under regulated flow rate (see Fig. S12). The hydrodynamic diameter obtained in this way at 0.01 M ionic strength was 38 ± 2 nm, which agrees with the theoretical data predicted for the average molar mass of the chitosan sample.
The hydrodynamic diameter data acquired above from DLS and OWLS can also be used to determine the electrokinetic charge of chi­tosan molecules, an essential parameter, which has not been before determined in the literature. This additionally requires the electropho­retic mobility of molecules p.e (this parameter is the ratio of the molecule migration velocity to the applied electric field) which can be directly measured by the LDV method as described above. The dependence of )ie on pH acquired at 0.01 M ionic strength and the temperature of 298 K is shown in Fig. 6. As can be noticed, the mobility attains a maximum value of 5.1 ^m cm(Vs) 1 at pH 2 and monotonically decreases to zero at pH ca. 8.5.
Using the experimental electrophoretic mobility )ie and the hydro­dynamic diameter one can determine the electrokinetic charge at the chitosan molecule by applying the Lorentz-Stokes relationship (Adamczyk et al., 2006); (Michna et al., 2017):
kT
qe = Innd^e = D^e	(10)
Consequently, the number of elementary charges Nc per one
molecule can be calculated as
Nc = qe/e, where e is the elementary charge 1.602 x 10 19 C.
Eq. (10) is valid for an arbitrary charge distribution and the shape of molecules. However, its accuracy decreases for larger ionic strengths where the double-layer thickness k 1 = (ekT/2e2I)1/2 (where e is the electric permittivity of the solvent) becomes comparable with the molecule diameter.
Using the experimental hydrodynamic diameter of 19 nm (for the molecule molar mass of 50 kDa) and the electrophoretic mobility data one obtains Nc = 50, 33 and 9 at pH 2, 5.6 and 7.3, respectively. The dependence of Nc on pH is graphically shown in Fig. 6. Analogously, for the average molar mass of 120 kDa where the hydrodynamic diameter is 40 nm one obtains Nc = 105, 69 and 19 at pH 2, 5.6 and 7.3, respec­tively. Considering that DP was 280 and 670 (for 50 and 120 kDa, respectively) and DA = 40% one can calculate that the electrokinetic charge at pH 2 amounts to 0.32 to 0.26 of the nominal charge (158 e and 402 e for 50 and 120 kDa, respectively). These results indicate that the molecule charge stemming from the protonated -NH2 groups is signifi­cantly compensated by counterion accumulation in the diffuse part of the electric double-layer. This effect is well-known as the Manning ion condensation (Manning, 1979). It is also interesting to mention that such behaviour was previously reported for PDADMAC (Adamczyk et al., 2014), and PLL (Adamczyk et al., 2018) macroions.
Except for the electrokinetic charge, the electrophoretic mobility data allow to calculate the zeta potential, an important parameter controlling macromolecule interactions among themselves, i.e., their solution stability, and their interactions with interfaces, i.e., the adsorption kinetics and isotherms. The dependence of the chitosan molecule zeta potential on pH calculated from the electrophoretic mobility using the general Ohshima model is plotted in Fig. 7. The electrophoretic mobility, the zeta potential and the number of electro- kinetic charges of the chitosan molecule at various pHs were presented in Table S4.
Furthermore, the dependences of zeta potential and the electroki- netic charge of the chitosan molecule on the temperature at pH = 2 for I = 0.01 M HCl were determined. The obtained results can be found in Fig. S11 and Table S5.
## 4. Viscosity measurements
Thorough characteristics of chitosan solutions were also acquired applying the viscosity method, widely used in the literature to determine

Fig. 7. Dependence of the zeta potential of the chitosan molecule on pH. Measurements conditions: I = 0.01 M; T = 298 K; bulk solution concentration 300 mg T. 1. The solid line denotes the logistic fit of experimental data.

the molar mass via the Mark-Houvink equation and other derivative parameters such as the chain conformation, persistence length, chain stiffness, etc. (Kasaai, 2007; Morris et al., 2009; Weinhold & Thoming, 2011) Primarily, in the measurements, the zero shear rate dynamic viscosity of dilute chitosan solution denoted as ns was measured for various pHs and temperatures at a fixed ionic strength of 0.01 M. These primary results were expressed as the dependence of the normalized viscosity ns/ne (where ne is the supporting electrolyte viscosity) on the chitosan volume fraction	= Cb/pp rather than on the mass fraction as
usually done in the literature.
Such dependencies of the normalized viscosity, ns/ne on the volume fraction ^v for various pHs, the temperature 298 K and I = 0.01 M are presented in Fig. 8. The dependencies of normalized viscosity on the volume fraction for various temperatures, at pH 2 are presented in Fig. S13.
It should be mentioned that dynamic viscosity measurements for

Fig. 8. Dependence of the normalized viscosity ns/ne on the volume fraction of chitosan solutions at various pHs, I = 0.01 M, T = 298 K. The lines represent linear interpolation of the experimental data.
other ionic strength were less reproducible because of the instability of chitosan solutions. To be more precise, due to the lower solubility of chitosan in less concentrated solutions of HCl, the range of ^v presented in Fig. 8 is inaccessible under HCl concentration lower than 6 x 10 3 M, as determined experimentally. Additionally, the direct dilution of freshly prepared chitosan solution in 0.01 M HCl was applied to prepare chitosan solution of lower ionic strength. Unfortunately, this approach resulted in precipitation of chitosan. To the best of our knowledge, there is no available literature data concerning the dynamic viscosity of chi­tosan solutions characterized by ionic strength lower than 0.01 M.
The slopes of these dependencies give directly the experimental values of the intrinsic viscosity increment vexp (a dimensionless parameter) defined as
Vexp = [n]Pp	(11)
where [n] is the usually defined intrinsic viscosity expressed as dL g \ therefore, having the dimension of a specific volume.
It is determined that vexp was practically independent of pH for the range 2-4 (see Fig. 8) assuming an average value of 1150 ± 50. This value is slightly lower for pH 5, attaining a value of 1070 ± 30. How­ever, at pH 6, vexp markedly decreased assuming 860 ± 40 for the NaCl concentration of 0.01. Such large values of the viscosity increment, compared to the Einstein value of 2.5 pertinent to spherical (random coil) molecule conformation, unequivocally indicate that the chitosan molecule assumes largely extended conformation. This agrees with the above prediction derived from DLS and OWLS measurements.
The influence of the temperature on the viscosity increment at pH 2 and I = 0.01 M was also studied. The results shown in Fig. S14 and Table S6 confirmed that the increment decreased from 1150 ± 50 to 710 ± 30 for 293 and 323 K.
These viscosity increment data were interpreted in terms of theo­retical results derived in Ref. (Brenner, 1974) within the framework of low Reynolds number hydrodynamics. In this work, the intrinsic vis­cosity increment was analytically calculated for prolate spheroids characterized by the elongation parameter A up to 50. A broad range of the Peclet (Pe) number defining the significance of the hydrodynamic shear rate to the rotary diffusion coefficient of molecules was consid­ered. In the limit of zero Pe number (corresponding to negligible shear rate) the exact numerical results obtained for A » 1 were interpolated by the following analytical expression
A2	A2
V = Clvln2A - 0.5 + C2vln2A - 1.5 + C	(12)
where c1v = 3/15, c2v = 1/15 and cv is 8/5 for spheroids and 14/15 for blunt cylinders (Harding, 1995).
The precision of Eq. (12) is ca. 1% for A = 10 and 0.2% for A above 100.
However, one should underline that Eq. (12) is strictly valid for rigid bodies having regular shape such as prolate spheroids or cylinders of arbitrary cross-section area. No exact theoretical results were reported in the literature for flexible, worm-like, molecule shapes. However, there exist results for cyclic molecule chains approximated by strings of touching beads, either freely jointed or forming Gaussian rings, with a quasi-toroidal geometry (Bernal et al., 2002). The obtained results were expressed as the ratio of the intrinsic viscosity increment of the linear to the cyclic chains having the same number of beads, denoted as qn. For the number of beads exceeding 20 (this corresponds to the A parameter in the slender body nomenclature), it is shown that qn was 0.60 ± 0.2. This result confirms that the increment of a flexible molecule bent to a form of a torus (a circle in the limit of large elongations) amounts to 60% of the molecule forming a fully expanded conformation. Therefore, it is reasonable to assume that any intermediate conformation such as example a semi-circle will produce even a smaller, about 20% change in the viscosity increments. By virtue of these results, one can calculate the limiting viscosity increment for a flexible molecule in the toroidal
conformation by multiplying the viscosity derived from Eq. (12) by the factor qn. Theoretical results calculated in this way are given in Table 2 and compared with the experimental value determined in this work for 0.01 M ionic strength. As can be seen, the experimental value of 1150 ± 50 agrees with the theoretically predicted 1090, which was calculated for a straight molecule conformation and the molar mass of 50 kDa, whereas the toroidal conformation yields vc = 660, i.e., significantly smaller. In contrast, for the average molar mass of 120 kDa, the theo­retical values of the viscosity increment for the straight and toroidal conformation are 4590 and 2760, respectively, which significantly ex­ceeds the experimental value. A plausible explanation of this discrep­ancy is the uncertainty in the molar mass determination, mainly caused by the presence of aggregates exhibiting significantly larger molar mass than the average value. As shown by Anthonsen et al. (Anthonsen et al., 1993) and Korchagina & Philippova (Korchagina & Philippova, 2010) such aggregates exhibit a compact molecule shape rather than largely elongated, pertinent to monomer molecules. As a result, although they shift the average molar mass to large values, they little contribute to the intrinsic viscosity. In order to test this hypothesis, some literature data acquired for well-defined experimental conditions are theoretically analyzed in terms of the hydrodynamic model using the molecule di­mensions derived from this work from the MD modeling.
Errington et al. (Errington et al., 1993) carried out measurements for chitosan samples of various origins characterized by molar mass deter­mined by the sedimentation equilibrium varying between 4.3 and 64 kDa and the acetylation degree of 58%. The ionic strength of the solution was 0.2 M and pH was 4.3. In contrast to other works, the density of the chitosan sample 1.72 g cm 3 was determined by the dilution method. The viscosity increment results shown in Table 2 indicate that an almost quantitative agreement with theoretical predictions is observed for the 28.9 and 64 kDa samples. However, for the low molar mass samples of 8.8 and 4.3 kDa, the experimental intrinsic viscosity increments were significantly larger than those predicted for a fully extended chain. This unusual behaviour can be attributed to the large uncertainty in the molar mass determination by the sedimentation equilibrium for low molar mass samples.
Anthonsen et al. (1993), performed systematic viscosity measure­ments for chitosan samples characterized by the molar mass (deter­mined by osmotic pressure) varying between 15 and 310 kDa and acetylation degrees 60, 15 and 0%, respectively. Additionally, the in­fluence of ionic strength changed between 1 and 0.013 M (at pH 5) was determined. In Table 2, the results obtained for DA = 15% and 0.013 M extrapolated to 0.01 M ionic strength are compared with the theoretical predictions derived from our model assuming pp = 1.72 g cm 3 that corresponds to the experimental value determined by Errington et al. (1993). Considering the possible experimental error, a satisfactory
Mp [kDa]	DP / [1]	Lext Rg [nm]	^ext / [1]	L01 / Rg [nm]	Л01 / [1]	Vext / [1]	V01 / [1]	Vc / [1]	[1]	Refs, Remarks
50	280	128	175	105	141	1610	1090	660	1150 ± 50	This work, DA = 40%
		37.0		30.3						M1 = 0.179 kg mol 1 / Pp = 1.5 g cm 3 pH 2-4, 0.01 M HCl
										T = 298 K
120	670	308	420	252	312	7910	4590	2760	1150	This work
		88.9		72.7
125	748	344	469	282	348	9680	5600	3360	2100	Anthonsen et al. (1993)
		99.3		81.4						DA = 15%,
98	587	270	368	222	274	6210	3630	2180	1900	M1 = 0.167 kg mol 1
		77.9		64.1						pH 5, 0.01 M NaCl
82	491	226	308	186	229	4490	2620	1570	1370	T = 295 K,
		65.2		53.7						Pp = 1.72 g cm-3 (assumed)
78	467	215	293	176	218	4100	2400	1490	1250
		62.1		50.8
62	371	171	233	140	173	2700	1580	948	1030
		49.4		40.4
35	210	96.4	132	79.1	98.2	973	575	344	550
		27.8		22.8
120	714	329	448	270	333	8900	5170	3100	403	Tsaih and Chen (1999)
		95.0		77.9						DA = 17%,
78	464	214	292	176	217	4070	2380	1430	217	M1 = 0.168 g mol_ 1
		61.8		50.8						Pp = 1.72 g cm-3 (assumed)
										T = 303 K
64.1	347	160	218	132	162	2400	1400	842	1380	Errington et al. (1993)
		46.2		38.1						DA = 58%,
28.9	156	71.9	98.0	59.0	72.9	572	340	203	193	M1 = 0.185 g mol 1
		20.8		17.0						Pp = 1.72 g cm 3
8.8	47.6	21.9	29.9	18.0	22.2	74	45	27	115	pH 4.3, 0.2 M NaCl
		6.3		5.2						T = 298 K
4.3	23.2	10.7	14.6	8.8	11.0	24	16	9.2	45
		3.1		2.5

Table 2
Theoretical (derived from the slender body approach) and experimental values of the intrinsic viscosity increments of chitosan molecules in aqueous electrolyte solutions.
DP = Mp/M1 - degree of polymerization the molecule.
Lext = DPlm - extended contour length of the molecule
7ext = Lext/dex - aspect ratio parameter.
701 = ^ext(dex/d01)3 - aspect ratio parameter for 0.01 M electrolyte
vext = viscosity increment for fully extended chain, Eq. (12).
v01 = fv (701) - viscosity increment for a cylinder and a spheroid valid for Л > 10.
vc = Cc fv U01) - viscosity increments for a cyclic molecule (Bernal et al., 2002) determined for 0.01 M electrolye. vexp = [tf]Pp - experimental viscosity increment.
lm = 0.460 nm; dex = 0.733 nm; lm01 = 0.378 nm; d01 = 0.809 nm (Table 1).

 agreement with theoretical predictions is evident for the molar mass range of 35 to 98 kDa. Only for the 125 kDa sample, the experimental intrinsic viscosity increment becomes markedly smaller than the theo­retical value predicted for the toroidal conformation of the molecules. One can argue that this deviation can be attributed to the uncertainty in the molar mass determination by the osmotic pressure measurements. It may become significant for molar mass above 100 kDa given that the concentration of chitosan in the osmotic pressure measurements attained 6000 mg L 1, increasing interactions among molecules, which may lead to aggregation.
The significant role of chitosan solutions aggregation creating un­certainty in molar mass determination is confirmed in other works. Thus, Tsaih and Chen (1999) performed systematic measurements of chitosan solution viscosity for samples characterized by molar mass determined by static light scattering varying between 78 and 914 kDa, and the acetylation degree of 17%, (at pH 2.18). The influence of ionic strength changed between 0.01 and 0.2 M at the temperature of 30 was investigated. In Table 2 the experimental results obtained for 78 and 120 kDa samples are compared with the theoretical predictions derived from our model assuming pp = 1.72 g cm 3. As can be inferred, the intrinsic viscosity increment for the molar mass of 120 kDa is almost eight times smaller than that theoretically predicted and more than four times smaller than the experimental value obtained by Anthonsen et al. (1993). For the molar mass of 78 kDa the increment is six times smaller than that obtained by Anthonsen for practically the same experimental conditions. The results obtained by Tsaih and Chen (1999) were inter­preted in terms of the Mark-Houwink (MH) equation. For 0.01 M ionic strength, the a and K parameters were 0.715 and 5.48 x 10 4 dL g ~1, respectively.
## 5. Conclusions
Extensive MD modeling confirmed that the chitosan molecule ex­hibits in electrolyte solutions a flexible-rod shape showing no tendency to the formation of helical conformation. Several parameters of primary significance were theoretically calculated for the first time such as the monomer contour length, the hydrated chain diameter and the molecule density under different ionic strengths. Applying an extrapolation pro­cedure these data enabled to calculate the contour length for chitosan molecules of various molar masses and the molecule length to diameter ratio. Considering that the latter parameter assumes large values, the molecule hydrodynamic diameter, gyration radius and the intrinsic viscosity increments were calculated by applying the slender body hy­drodynamics. It was predicted that the hydrodynamic diameter for straight and bent molecule conformation was practically equal, whereas the increment decreased by ca. 40% for the toroidal molecule confor­mation. These theoretical results allowed to quantitatively interpret experimental measurements, where the diffusion coefficient, the hy­drodynamic diameter, the electrophoretic mobility and the intrinsic viscosity increment of the chitosan molecule were determined at a broad range of pH and the temperature. A satisfactory agreement was attained considering the sample dispersity.
Additionally, a thorough analysis of extensive literature data ac­quired under well-defined experimental conditions confirmed the utility of the hydrodynamic model developed in this work for predicting intrinsic viscosity of lower molar mass chitosan solutions.
It is argued that besides significance for basic science as reference data, the obtained results can be exploited for the optimization of pro­cedures for macroion film formation at various substrates often used as efficient supports for bioparticle immobilization.
## CRediT authorship contribution statement
Dawid Lupa: Investigation, Methodology, Visualization, Writing - original draft, Writing - review & editing. Wojciech Plazinski: Inves­tigation, Methodology, Visualization, Writing - original draft, Writing - review & editing. Aneta Michna: Investigation, Methodology, Writing - review & editing, Funding acquisition. Monika Wasilewska: Investi­gation, Methodology, Writing - original draft. Paweł Pomastowski: Investigation, Methodology, Writing - original draft. Adrian Gołę­biowski: Investigation, Methodology, Writing - original draft. Bogu­sław Buszewski: Conceptualization, Writing - review & editing, Data curation. Zbigniew Adamczyk: Conceptualization, Writing - original draft, Writing - review & editing, Supervision.
## Declaration of competing interest
The authors declare that they have no known competing financial interests or personal relationships that could have appeared to influence the work reported in this paper.
## Acknowledgments
This work was financially supported by the National Science Centre, Poland, Opus Project, UMO-2018/31/B/ST8/03277 and partially by the Statutory activity of the J. Haber Institute of Catalysis and Surfa­ceChemistry PAS (advanced calculation for interpretation of experi­mental data).
Paweł Pomastowski, Adrian Gołębiowski and Bogusław Buszewski are members of Torun Center of Excellence “Towards Personalized Medicine” operating under Excellence Initiative-Research University.
## Appendix A. Supplementary data
Supplementary data to this article can be found online at https://doi. org/10.1016/j.carbpol.2022.119676.
## References
Abraham, M. J., Murtola, T., Schulz, R., Pall, S., Smith, J. C., Hess, B., & Lindahl, E. (2015). GROMACS: High performance molecular simulations through multi-level parallelism from laptops to supercomputers. SoftwareX, 1-2, 19-25. https://doi.org/ 10.1016/j.softx.2015.06.001
Adamczyk, Z., Bratek, A., Jachimska, B., Jasinski, T., & Warszynski, P. (2006). Structure of poly(acrylic acid) in electrolyte solutions determined from simulations and viscosity measurements. Journal of Physical Chemistry B, 110(45), 22426-22435. https://doi.org/10.1021/jp063981w
Adamczyk, Z., Cichocki, B., Ekiel-Jez ewska, M. L., Słowicka, A., Wajnryb, E., & Wasilewska, M. (2012). Fibrinogen conformations and charge in electrolyte solutions derived from DLS and dynamic viscosity measurements. Journal of Colloid and Interface Science, 385(1), 244-257. https://doi.org/10.1016/j.jcis.2012.07.010
Adamczyk, Z., Jamrozy, K., Batys, P., & Michna, A. (2014). Influence of ionic strength on poly(diallyldimethylammonium chloride) macromolecule conformations in electrolyte solutions. Journal of Colloid and Interface Science, 435, 182-190. https:// doi.org/10.1016/j.jcis.2014.07.037
Adamczyk, Z., Morga, M., Kosior, D., & Batys, P. (2018). Conformations of poly-l-lysine molecules in electrolyte solutions: Modeling and experimental measurements.
Journal of Physical Chemistry C, 122(40), 23180-23190. https://doi.org/10.1021/ acs.jpcc.8b07606
Adamczyk, Z., Batys, P., Płazmski, W., Morga, M., Lupa, D., & Michna, A. (2021). Macroion molecule properties from slender body hydrodynamics. Polymers for Advanced Technologies, 32(10), 3900-3908. https://doi.org/10.1002/PAT.5319
Anthonsen, M. W., Várum, K. M., & Smidsr0d, O. (1993). Solution properties of chitosans: Conformation and chain stiffness of chitosans with different degrees of N- acetylation. Carbohydrate Polymers, 22(3), 193-201. https://doi.org/10.1016/0144- 8617(93)90140-Y
Bano, I., Arshad, M., Yasin, T., & Ghauri, M. A. (2019). Preparation, characterization and evaluation of glycerol plasticized chitosan/PVA blends for burn wounds.
International Journal of Biological Macromolecules, 124, 155-162. https://doi.org/
10.1016/j.ijbiomac.2018.11.073
Barducci, A., Bussi, G., & Parrinello, M. (2008). Well-tempered metadynamics: A smoothly converging and tunable free-energy method. Physical Review Letters, 100 (2), Article 020603. https://doi.org/10.1103/PhysRevLett.100.020603
Bernal, J. M. G., Tirado, M. M., Freire, J. J., & García De La Torre, J. (2002). Monte Carlo calculation of hydrodynamic properties of cyclic polymers in ideal solution. Macromolecules, 23(13), 3357-3362. https://doi.org/10.1021/MA00215A024
Berth, G., & Dautzenberg, H. (2002). The degree of acetylation of chitosans and its effect on the chain conformation in aqueous solution. Carbohydrate Polymers, 47(1), 39-51. https://doi.org/10.1016/S0144-8617(00)00343-X
Boardman, S. J., Lad, R., Green, D. C., & Thornton, P. D. (2017). Chitosan hydrogels for targeted dye and protein adsorption. Journal of Applied Polymer Science, 44846. https://doi.org/10.1002/app.44846

Brenner, H. (1974). Rheology of a dilute suspension of axisymmetric brownian particles. International Journal of Multiphase Flow, 1(2), 195-341. https://doi.org/10.1016/ 0301-9322(74)90018-4
Bussi, G., Donadio, D., & Parrinello, M. (2007). Canonical sampling through velocity rescaling. The Journal of Chemical Physics, 126(1), Article 014101. https://doi.org/ 10.1063/1.2408420
Chien, R. C., Yen, M. T., & Mau, J. L. (2016). Antimicrobial and antitumor activities of chitosan from shiitake stipes, compared to commercial chitosan from crab shells. Carbohydrate Polymers, 138, 259-264. https://doi.org/10.1016/j. carbpol.2015.11.061
Colfen, H., Berth, G., & Dautzenberg, H. (2001). Hydrodynamic studies on chitosans in aqueous solution. Carbohydrate Polymers, 45(4), 373-383. https://doi.org/10.1016/ S0144-8617(00)00269-1
Czechowska-Biskup, R., Wojtasz-Paj^k, A., Sikorski, J., Henke, A., Ulanski, P., & Rosiak, J. M. (2007). Aqueous solutions of hydrochloric acid as simple solvents of chitosan for viscosity- and light-scattering-based molecular weight determination. Polish Chitin Society, 87-94.
Darden, T., York, D., & Pedersen, L. (1998). Particle mesh Ewald: An N-log(N) method for Ewald sums in large systems. The Journal of Chemical Physics, 98(12), 10089. https:// doi.org/10.1063/1.464397
Earl, D. J., & Deem, M. W. (2005). Parallel tempering: Theory, applications, and new perspectives. Physical Chemistry Chemical Physics, 7(23), 3910-3916. https://doi. org/10.1039/B509983H
Einstein, A. (1908). Elementare theorie der brownschen 1) bewegung. Zeitschrift für Elektrochemie und Angewandte Physikalische Chemie, 14(17), 235-239. https://doi. org/10.1002/bbpc.19080141703
Errington, N., Harding, S. E., Varum, K. M., & Illum, L. (1993). Hydrodynamic characterization of chitosans varying in degree of acetylation. International Journal of Biological Macromolecules, 15(2), 113-117. https://doi.org/10.1016/0141-8130(93) 90008-A
Gonzalez-Espinosa, Y., Sabagh, B., Moldenhauer, E., Clarke, P., & Goycoolea, F. M. (2019). Characterisation of chitosan molecular weight distribution by multi­detection asymmetric flow-field flow fractionation (AF4) and SEC. International Journal of Biological Macromolecules, 136, 911-919. https://doi.org/10.1016/j. ijbiomac.2019.06.122
Guvench, O., Mallajosyula, S. S., Raman, E. P., Hatcher, E., Vanommeslaeghe, K., Foster, T. J., Jamison, F. W., & Mackerell, A. D. (2011). CHARMM additive all-atom force field for carbohydrate derivatives and its utility in polysaccharide and carbohydrate A protein modeling. Journal of Chemical Theory and Computation, 7 (10), 3162-3180. https://doi.org/10.1021/ct200328p
Harding, S. E. (1995). On the hydrodynamic analysis of macromolecular conformation. Biophysical Chemistry, 55(1-2), 69-93. https://doi.org/10.1016/0301-4622(94) 00143-8
Harding, S. E., Tombs, M. P., Adams, G. G., Paulsen, B. S., Inngjerdingen, K. T., & Barsett, H. (2017). Marine polysaccharides. In S. E. Harding, M. P. Tombs, G. G. Adams, B. S. Paulsen, K. T. Inngjerdingen, & H. Barsett (Eds.), An introduction to polysaccharide biotechnology (2nd ed., pp. 153-192). Taylor & Francis Group.
Hasegawa, M., Isogai, A., & Onabe, F. (1994). Molecular mass distribution of chitin and chitosan. Carbohydrate Research, 262(1), 161-166. https://doi.org/10.1016/0008- 6215(94)84013-X
Hess, B. (2008). P-LINCS: A parallel linear constraint solver for molecular simulation. Journal of Chemical Theory and Computation, 4(1), 116-122. https://doi.org/ 10.1021/ct700200b
Hockney, R. (1970). The potential calculation and some applications. In B. Alder, S. Fernbach, & M. Rotenberg (Eds.), Methods in computational physics (pp. 135-211).
Jorgensen, W. L., Chandrasekhar, J., Madura, J. D., Impey, R. W., & Klein, M. L. (1998). Comparison of simple potential functions for simulating liquid water. The Journal of Chemical Physics, 79(2), 926. https://doi.org/10.1063/1.445869
Kaczmarek, M. B., Struszczyk-Swita, K., Li, X., Szcz^sna-Antczak, M., & Daroch, M. (2019). Enzymatic modifications of chitin, chitosan, and chitooligosaccharides. Frontiers in Bioengineering and Biotechnology, 7, 243. https://doi.org/10.3389/ fbioe.2019.00243
Kasaai, M. R. (2007). Calculation of Mark-Houwink-Sakurada (MHS) equation viscometric constants for chitosan in any solvent-temperature system using experimental reported viscometric constants data. Carbohydrate Polymers, 68(3), 477-488. https://doi.org/10.1016/j.carbpol.2006.11.006
Korchagina, E. V., & Philippova, O. E. (2010). Multichain aggregates in dilute solutions of associating polyelectrolyte keeping a constant size at the increase in the chain length of individual macromolecules. Biomacromolecules, 11(12), 3457-3466. https://doi.org/10.1021/bm100990u
Lamarque, G., Lucas, J. M., Viton, C., & Domard, A. (2005). Physicochemical behavior of homogeneous series of acetylated chitosans in aqueous solution: Role of various structural parameters. Biomacromolecules, 6(1), 131-142. https://doi.org/10.1021/ bm0496357
Manning, G. S. (1979). Counterion binding in polyelectrolyte theory. Accounts of
Chemical Research, 12(12), 443-449. https://doi.org/10.1021/ar50144a004
Mansfield, M. L., & Douglas, J. F. (2008). Transport properties of rodlike particles. Macromolecules, 41(14), 5422-5432. https://doi.org/10.1021/ma702839w
Meng, X., Liu, H., Dong, X., Wang, Q., Xia, Y., & Hu, X. (2022). A soft Pickering emulsifier made from chitosan and peptides endows stimuli-responsiveness, bioactivity and biocompatibility to emulsion. Carbohydrate Polymers, 277, Article 118768. https:// doi.org/10.1016/j.carbpol.2021.118768
Michna, A., Adamczyk, Z., Sofinska, K., & Matusik, K. (2017). Monolayers of poly(amido amine) dendrimers on mica - In situ streaming potential measurements. Journal of Colloid and Interface Science, 485, 232-241. https://doi.org/10.1016/j. jcis.2016.09.007
Michna, A., Pomorska, A., Nattich-Rak, M., Wasilewska, M., & Adamczyk, Z. (2020). Hydrodynamic solvation of poly(amido amine) dendrimer monolayers on silica. Journal of Physical Chemistry C, 124, 17684-17695. https://doi.org/10.1021/acs. jpcc.0c04638
Michna, A., Piazinski, W., Lupa, D., Wasilewska, M., & Adamczyk, Z. (2021). Carrageenan molecule conformations and electrokinetic properties in electrolyte solutions: Modeling and experimental measurements. Food Hydrocolloids, 121, Article 107033. https://doi.org/10.1016/j.foodhyd.2021.107033
Miyamoto, S., & Kollman, P. A. (1992). Settle: An analytical version of the SHAKE and RATTLE algorithm for rigid water models. Journal of Computational Chemistry, 13(8), 952-962. https://doi.org/10.1002/jcc.540130805
Morris, G. A., Castile, J., Smith, A., Adams, G. G., & Harding, S. E. (2009). Macromolecular conformation of chitosan in dilute solution: A new global hydrodynamic approach. Carbohydrate Polymers, 76(4), 616-621. https://doi.org/ 10.1016/j.carbpol.2008.11.025
Ohshima, H. (2012). Electrophoretic mobility of charged particles. In H. Ohshima (Ed.), Electrical phenomena at interfaces and biointerfaces: Fundamentals and applications in nano-, bio-, and environmental sciences (1st ed., pp. 35-49). John Wiley & Sons Inc.
Park, S., Lee, J., Qi, Y., Kern, N. R., Lee, H. S., Jo, S., Joung, I., Joo, K., Lee, J., & Im, W. (2019). CHARMM-GUI Glycan Modeler for modeling and simulation of carbohydrates and glycoconjugates. Glycobiology, 29(4), 320-331. https://doi.org/ 10.1093/glycob/cwz003
Parrinello, M., & Rahman, A. (1981). Polymorphic transitions in single crystals: A new molecular dynamics method. Journal of Applied Physics, 52(12), 7182-7190. https:// doi.org/10.1063/1.328693
Patrulea, V., Ostafe, V., Borchard, G., & Jordan, O. (2015). Chitosan as a starting material for wound healing applications. European Journal of Pharmaceutics and Biopharmaceutics, 97, 417-426. https://doi.org/10.1016/j.ejpb.2015.08.004
Pini, N. I. P., Lima, D. A. N. L., Luka, B., Ganss, C., & Schlueter, N. (2020). Viscosity of chitosan impacts the efficacy of F/Sn containing toothpastes against erosive/ abrasive wear in enamel. Journal of Dentistry, 92, Article 103247. https://doi.org/ 10.1016/j.jdent.2019.103247
Raguzzoni, J. C., Delgadillo, I., & Lopes da Silva, J. A. (2016). Influence of a cationic polysaccharide on starch functionality. Carbohydrate Polymers, 150, 369-377. https://doi.org/10.1016/j.carbpol.2016.05.024
Rajabi, M., McConnell, M., Cabral, J., & Ali, M. A. (2021). Chitosan hydrogels in 3D printing for biomedical applications. Carbohydrate Polymers, 260, Article 117768. https://doi.org/10.1016/j.carbpol.2021.117768
Rinaudo, M., Milas, M., & Dung, P. L. (1993). Characterization of chitosan. Influence of ionic strength and degree of acetylation on chain expansion. International Journal of Biological Macromolecules, 15(5), 281-285. https://doi.org/10.1016/0141-8130(93) 90027-J
Saha, D., & Bhattacharya, S. (2010). Hydrocolloids as thickening and gelling agents in food: A critical review. Journal of Food Science and Technology, 47(6), 587-597. https://doi.org/10.1007/s13197-010-0162-6
Schatz, C., Viton, C., Delair, T., Pichot, C., & Domard, A. (2003). Typical physicochemical behaviors of chitosan in aqueous solution. Biomacromolecules, 4(3), 641-648. https://doi.org/10.1021/bm025724c
Singhal, A., Schneible, J. D., Lilova, R. L., Hall, C. K., Menegatti, S., & Grafmuller, A. (2020). A multiscale coarse-grained model to predict the molecular architecture and drug transport properties of modified chitosan hydrogels. Soft Matter, 16(47), 10591-10610. https://doi.org/10.1039/d0sm01243b
Soares, L.d. S., Perim, R. B., de Alvarenga, E. S., Guimaraes, L.d. M., Teixeira, A. V. N. d. C., Coimbra, J. S.d. R., & de Oliveira, E. B. (2019). Insights on physicochemical aspects of chitosan dispersion in aqueous solutions of acetic, glycolic, propionic or lactic acid. International Journal of Biological Macromolecules, 128(1), 140-148. https://doi.org/10.1016/j.ijbiomac.2019.01.106
Suo, H., Zhang, J., Xu, M., & Wang, L. (2021). Low-temperature 3D printing of collagen and chitosan composite for tissue engineering. Materials Science and Engineering C, 123, Article 111963. https://doi.org/10.1016/j.msec.2021.111963
Tribello, G. A., Bonomi, M., Branduardi, D., Camilloni, C., & Bussi, G. (2014). PLUMED 2: New feathers for an old bird. Computer Physics Communications, 185(2), 604-613. https://doi.org/10.1016/j.cpc.2013.09.018
Tsaih, M. L., & Chen, R. H. (1999). Effects of ionic strength and pH on the diffusion coefficients and conformation of chitosans molecule in solution. Journal of Applied Polymer Science, 73(10), 2041-2050. https://doi.org/10.1002/(SICI)1097-4628 (19990906)73:10<2041::AID-APP22>3.0.CO;2-T
Tsereteli, L., & Grafmuller, A. (2017). An accurate coarse-grained model for chitosan polysaccharides in aqueous solution. PLoS ONE, 12(7), Article e0180938. https:// doi.org/10.1371/journal.pone.0180938
Vakili, M., Rafatullah, M., Salamatinia, B., Abdullah, A. Z., Ibrahim, M. H., Tan, K. B., Gholami, Z., & Amouzgar, P. (2014). Application of chitosan and its derivatives as adsorbents for dye removal from water and wastewater: A review. Carbohydrate Polymers, 113, 115-130. https://doi.org/10.1016/j.carbpol.2014.07.007
Wan Ngah, W. S., Teong, L. C., & Hanafiah, M. A. K. M. (2011). Adsorption of dyes and heavy metal ions by chitosan composites: A review. Carbohydrate Polymers, 83(4), 1446-1456. https://doi.org/10.1016/j.carbpol.2010.11.004
Wang, W., Bo, S., Li, S., & Qin, W. (1991). Determination of the Mark-Houwink equation for chitosans with different degrees of deacetylation. International Journal of Biological Macromolecules, 13(5), 281-285. https://doi.org/10.1016/0141-8130(91) 90027-R
Wardy, W., Pujols Martinez, K. D., Xu, Z., No, H. K., & Prinyawiwatkul, W. (2014). Viscosity changes of chitosan solution affect physico-functional properties and

consumer perception of coated eggs during storage. LWT - Food Science and
Technology, 55(1), 67-73. https://doi.org/10.1016/j.lwt.2013.07.013
Wasilewska, M., Adamczyk, Z., Pomorska, A., Nattich-Rak, M., & Sadowska, M. (2019).
Human serum albumin adsorption kinetics on silica: Influence of protein solution stability. Langmuir, 35(7), 2639-2648. https://doi.org/10.1021/acs. langmuir.8b03266
Weinhold, M. X., & Thoming, J. (2011). On conformational analysis of chitosan.
Carbohydrate Polymers, 84(4), 1237-1243. https://doi.org/10.1016/j. carbpol.2011.01.011