Top Catal (2013) 56:745–749 DOI 10.1007/s11244-013-0026-1
Influence of Potassium and NO Addition on Catalytic Activity
in Soot Combustion and Surface Properties of Iron and Manganese Spinels
Piotr Legutko•Wojciech Kaspera•Tomasz Jakubek•Paweł Stelmachowski•AndrzejKotarba
Published online: 18 April 2013
©The Author(s) 2013. This article is published with open access at Springerlink.com
Abstract Two series of (0–4 wt%) potassium doped oxide catalystsbasedonironandmanganesespinelwereprepared. The synthesized materials were characterized in terms of their structure (XRD, Raman spectroscopy) and surface electronic properties (work function measurements). The catalytic activity towards soot combustion was determined bytemperatureprogrammedoxidationofaphysicalmixture of soot and catalyst intight contactin gas oxygen mixtures with and without NO addition. For iron spinel based mate- rials, where potassium is localized at the surface, the cata- lytic activity correlates with the work function lowering uponKdoping,whileformanganesespinelbasedmaterials, where potassium is incorporated into the bulk (formationof KMn4O8or KMn8O16), the correlation was not found. The presence of NO in the gas mixture leads to a systematic decrease of soot ignition temperature for allsamples.
burned. Typical size of soot particles/aggregates between 50 and 500 nm, is large enough to be harmful for human health. Soot has also been proven to have carcinogenic and mutagenic properties [1]. Jacobson [2], from Stanford University, claims in‘‘Journalof GeophysicalResearch’’that soot pollution is one of the main negative influences causing climate change (global warming). Soot being emitted by factories can stay aloft in the air for as long as a dozen weeks, creating an aerosol which absorbs solar radiation, which can have a direct effect on the climate. According to Jacobson’s calculations, the lowering of soot emissions into the atmosphere would cause the lowering of yearly temperatures by 1°C in 15 years. Soot, which has settled on the surface of ice, lowers the ability of the ice to reflectsolarlight—partofthesolarradiationisabsorbedby the soot and converted into thermal energy. An atmosphere content of a few parts per billion is enough for the settling soot to change the snows reflecting ability by 1 %. This phenomenon has negative consequences for the climate, since such interference into the global energy balance couldresultinariseintemperature.
To prevent human illness and climate change soot must be removed or its emissions stopped. Several ways have been developed for this purpose. Reactors or engines may be designed to prevent the formation of soot, yet this method has technological hindrances. On the other hand soot may be removed by use of filters. A disadvantage of this method is that the filters must be replaced and the soot is not permanently eliminated. A third method is to use a catalyst which would lower the temperature of ignition of soot, triggering its combustion in the reactor [3].
Existing catalysts are either ineffective or based on expensive noble metals. One of such catalysts is based on platinum applied to a cerium–zirconium support. The cat- alyst is based on technology which places a catalytically
Keywords Soot combustion·Iron·Manganese·Spinel·
Potassium
1 Introduction
Soot is a product of the incomplete combustion of hydro- carbons, coal or other such materials, comprised of various arrangements of carbon molecules. The composition of sootdependshighlyontheconditionsandsubstancebeing
P. Legutko·W. Kaspera·T. Jakubek·P. Stelmachowski·
A. Kotarba (&)
Faculty of Chemistry, Jagiellonian University, Ingardena 3,30-060Krako´w,Poland
e-mail:kotarba@chemia.uj.edu.pl
P. Legutko
e-mail:legutko@chemia.uj.edu.pl
13
ORIGINAL PAPER

746
Top Catal (2013) 56:745–749
2.3 Soot Combustion Tests
active material on a diesel particulate filter (DPF) [3]. Promising substitutes are catalysts based on transition metals, which are relatively cheap and harmless to the environment. Oxides containing transition metals such as perovskite-type [4] and spinel-type [5] are being investi- gated intensively. Moreover, it is widely accepted that the catalytic activity of the material in the soot combustion process can be enhanced by alkali doping [6,7]. Nitrogenoxides are present in diesel exhaust fumes and some papers report that NO in particular has a positive effect on catalyst activity in soot combustion, as it forms NO2, which is a stronger oxidant for carbon particles than oxygen [8]. The aim of this study is to investigate how alkali doping influences the catalytic activity of iron and manganese oxides with a spinel structure in soot combustion. More- over, the effect of NO addition will also be addressed.
The activity of the catalysts in soot combustion was measured by means of temperature programmed reaction (TPR).Thequartzfixed-bedreactorwasheated(10°C/min) from RT to 900°C and two gas mixtures were used during the tests: 5 % O2in He, as well as 3.3 % O2, 0.3 % NO in He,bothata60ml/minflow.Thesamplesforthesoot
combustion tests were prepared by weighing 0.05 g of soot (Degussa–Printex80) and the catalyst in an 1:8 ratio and then grinding them in a mortar for 10 min following thetight contactmethod. The changes in the gas composition upon the soot oxidation reaction were monitored by a quadrupole mass spectrometer (SRS RGA200, lines form/z=46 (NO2), 44 (CO2), 32 (O2), 30 (NO), 28(CO),
18 (H2O)).
3 Results and Discussion
2 Experimental
The X-ray diffractograms prove the spinel structure of both iron [9] and manganese spinel materials [10], as shown in Fig.1. The diffractograms were indexed in theFd3mandPmabspace groups, respectively. In the case of iron oxide, both magnetite (Fe3O4) and maghemite (c-Fe2O3) crystalize with a spinel structure, thus, based on the XRD data, we cannot unambiguously determine the definite phase com- position.RamanspectraoftheinvestigatedironspinelbasedmaterialsareshowninFig.2.Thepeakat640cm-1orig-inates from magnetite (curvespinel) [11]. Wide peaks ataround190,350,500and700cm-1arecharacteristicfor
maghemite (circles), while narrow peaks at 225, 247, 299,412,498and613cm-1belongtohematite(diamonds).Pop-upandaevanescentnarrowpeakat690cm-1maybeassigned to a bipyramidal FeO5[12]. The presence of maghemite is not surprising since fine powdered magnetite easily undergoes oxidation, which may be induced by laser radiation during the measurement or due to calcination of potassium doped materials [13]. In the case of manganese spinel we observe peaks characteristic for Mn3O4[14] (curvea,Fig.3).Uponthepotassiumdopingandcalcination the structure of the sample changes and peakscharacteristic of cryptomelane-type manganese dioxide (circles) [15], as well asc-MnO2(diamonds) [16] and pyrolusiteb-MnO2(squares)[16]appear.Othermanganesecompounds,suchas birnessite (KMn4O8) exhibit peaks close to cryptomelane (KMn4O16) and spinel type compounds and thus it is diffi- cult to confirm or exclude the presence of thisphase.
The influence of potassium addition on the catalytic activity in soot oxidation for the iron spinel is shown in Fig.4(diamonds). The character of this dependence is similar to a Morse curve (steep slope, minimum and asymptote),whichbringstomindtheToppingmodelof
2.1 Catalyst Preparation
The catalysts were prepared by weighing 1 g of commer- cial spinel (Mn3O4and Fe3O4,Aldrich) and adding an appropriate amount of potassium carbonate solution to achieve the desired alkali loading (0–4 wt%). Afterwards, the catalysts were dried for 1 h at 100°C and subsequently
calcined at 400°C for 4 h.
2.2 Physicochemical Characterization
The Raman spectra were recorded at room temperature in ambient conditions using a Renishaw InVia spectrometer equipped with a Leica DMLM confocal microscope and a CCD detector, with an excitation wavelength of 785 nm. The laser power at the sample position was 1.5 or 3 mW (0.5 or 1 % of total power) with a magnification of 209. The Raman scattered light was collected in the spectralrangeof150–850cm-1.Atleast6scans,10seach,wereaccumulated to ensure a sufficient signal to noise ratio. XRD patterns were recorded by a Philips X’Pert APD powder diffractometer with Cu Karadiation at 10 mA and 10 kV, 2hstep scans of 0.02°and a counting time of 1 s per step. Electron donor properties (work function) of the samples were determined by Kelvin Probe (McAllister, KP6500). For each measurement 0.1 g of sample was pressed under 8 MPa for 1 min to form a pellet. Themeasurementwasperformedinavacuum(10-6mbar)at150°C after heating the sample to 400°C to standardize the catalyst surface. A stainless steel electrode (d=3 mm,U=4.1eV)wasusedasareference.
13

Top Catal (2013) 56:745–749
747
Fig. 1 Diffractograms of investigated spinel materials: Fe3O4and Mn3O4together with references [9,10]
Fig. 2 Raman spectra of potassium doped, iron oxide based samples: Fe3O4(a), potassium doped with 0.01 theoretical monolayers of K2CO3(b), 0.2 (c), 0.3 (d), 0.6 (e). Maghemite phase–circles, hematitephase–diamonds
Fig. 3 Raman spectra of potassium doped, manganese oxide based samples: Mn3O4(a), potassium doped with 0.5 theoretical monolay- ers of K2CO3(b), 3 (c), 4.5 (d), 6.5 (e), 11 (f)
surface alkali promotion [17]. It is reported that catalytic activity changes (especially in catalytic processes where the electronic factor plays a key role) are excused by this model [18]. This is also a typical dependence forsystems
where alkalis are located on the catalyst surface, forming surface dipoles [19].
The influence of NO addition on the catalytic activity is shown in Fig.4, (squares). The effect is beneficial and
13

748
Top Catal (2013) 56:745–749
Fig. 4 Influence of potassium promotion and NO addition (lowercurve) on ignition temperature of iron spinel
Fig. 6 Correlation of temperature of ignition and work function for K-doped iron (diamonds) and manganese (squares) oxide based catalysts
of NO does not induce any changes in its reactivity. This is in contrast to the redox and noble metal based catalysts where the NO addition usually enhances the catalytic activity [22].
The non-systematic effect for K doped Mn3O4, in con- trast to Fe3O4may be brought about by structural changes of the material as indicated by Raman spectroscopy (Fig.3). This nanostructurization of manganese oxide based materials by potassium, leading to the formation of a layered structure of KMn4O8and KMn4O16, is found to be the main factor responsible for the very high activity of these catalysts. The ignition temperature of potassium promoted manganese oxide catalysts can be as low as 250°C. In Fig.6the dependence between activity and electro-donor properties of iron (diamonds) and manganese (squares) spinels is shown. The work function of the iron spinel changes in a wide range upon K addition and the highest activity is observed for a potassium coverage of 0.5, which corresponds to the lowest work function value. This type of dependence of reactivity on the loading of alkali promoter is typical for a surface promotion [18]. The fact that mainly surface promotion is observed is caused by thehightemperaturesrequiredfortheformationofbulk
Fig. 5 Influence of potassium promotion and NO addition (lowercurve) on ignition temperature of manganese spinel
exhibitsasystematiccharacter(*30°C),butdisappearsnear the 1.5 monolayer coverage, which could be the result of full coverage of the catalyst surface by potassium car- bonate. The influence of potassium addition on the cata- lytic activity of the manganese spinel is shown in Fig.5(diamonds). This dependence is similar to that of the iron spinel, however, less pronounced. The influence ofNO
addition (squares) measures between 5°C (measurement error) and 25°C. It is worth mentioning that during the
catalytic tests for both series,m/z=46 was traced with mass spectrometer but no signal was detected, which indicates that NO2was not produced during the reaction. It indicates that NO acts directly as an oxidizing agent. This behavior is different from that observed for other oxide based catalysts during soot oxidation, where the formation of NO2is often postulated [20,21].
The minor effect of addition of NO for the catalystswith high potassium loading is related to the formation of sur- face potassium carbonate. Indeed, we found, that if pure K2CO3isusedasacatalystforsootoxidationtheaddition
potassium ferrite phases, which exceed 600°C
[23]. The
minimum of ignition temperature, shown in Fig.4, is related to the optimal dispersion of the surface potassium, which brings its highest promotional effect. This is asso- ciated with the formation of surface dipoles and resultant changes in the work function of the catalytic material (DU& 0.6 eV), much higher than for Mn based samples, (Fig.6). For manganese spinel the work function is rather independent on potassium addition (DU& 0.2 eV, Fig.6), suggesting that the promoter is incorporated into the bulk of the manganese oxide phase, as revealed by Raman spectroscopy (Fig.3). In this case, at thecalcination
13

Top Catal (2013) 56:745–749
749
temperature of 400°C, mixed potassium-manganese pha- ses can be already formed [24]. Thus, much higher potas-sium loading (per unit surface area) in comparison with theK/Fe3O4samples is necessary for formation of the surfaceK2CO3phase, (Fig.5).
References
1. van Setten BAAL, Makkee M, Moulijn JA (2001) Cat Rev 43:489–564
2. JacobsonMZ(2010)JGeophysResD115:24–31
3. Fino D (2007) Sci Technol AdvMater 8:93–100
4. UraB,Trawczyn´skiJ,KotarbaA,BieniaszW,Illan-GomezMJ,Bueno-Lo´pezA,Lo´pez-Sua´rezFE(2011)ApplCatal101:169–175
5. Fino D, Russo N, Saracco G, Specchia V (2006) J Catal242:38–47
6. AnH,McGinnPJ(2006)ApplCatal62:46–56
7. LegutkoP,StelmachowskiP,Tre˛balaM,SojkaZ,KotarbaA(2013) Top Catal 56:489–492.doi:10.1007/s11244-013-0003-8
8. KumarPA, Tanwar MD, Russo N, Pirone R, Fino D (2012) Catal Today184:279–287
9. Haavik C, Stolen S, Fjellvag H, Hanfland M, Hausermann D (2000) Am Minerol 85:514–523
10. Baron V, Gutzmer J, Rundlof H, Tellgren R (1998) Am Minerol 83:739–786
11. de Faria DLA, Venancio Silva S, de Oliveira MT (1997) JRaman Spectrosc28:873–878
12. Kreisel J, Lucazeau G, Vincent H (1998) J Solid State Chem 137:127–137
13. Shebanova ON, Lazor P (2003) J Raman Spectrosc34:845–852
14. HanY-F,ChenF,ZhongZ,RameshK,ChenL,WidjajaE(2006) J Phys Chem B110:24450–24456
15. GaoT,GlerupM,KrumeichF,NesperR,Fjellva˚gH,NorbyP(2008) J Phys Chem C112:13134–13140
16. Julien C, Massot M, Rangan S, Lemal M, Guyomard D (2002) J Raman Spectrosc33:223–228
17. Brison J, Mine N (2007) Surf Sci 601:1467–1472
1. Zasada F, Stelmachowski P, Maniak G, Paul J-F, Kotarba A, Sojka Z (2009) Catal Lett127:126–131
2. Verhoef RW, Asscher M (1997) SurfSci 391:11–18
3. Fino D, Russo N, Saracco G, Specchia V (2008) Powder Technol 180:74–78
4. Fino D, Russo N, Saracco G, Specchia V (2006) J Catal 242:38–47
5. Cauda E, Fino D, Saracco G, Specchia V (2004) Top Catal 30–31:299–304
6. Joseph Y, Ketteler G, Kuhrs C, Ranke W, Weiss W, Schlogl R (2001) Phys Chem Chem Phys3:4141–4153
7. AtribakI,Bueno-Lo´pezA,Garc´ıa-Garc´ıaA,NavarroP,Fr´ıasD,
Montes M (2010) Appl Catal 93:267–273
4 Conclusions
Two series of (0–4 wt%)
potassium promoted iron and
manganese spinel based catalysts were investigated in model soot oxidation processes. The temperatures of soot ignition for K-promoted iron spinels were found to be in the range of 320–360°C, while for K-promotedmanganese spinels,intherangeof250–300°C.Wefoundthatpres-
ence of NO in the gas feed leads to a decrease of the soot ignition temperature independently of the base metal oxide or potassium loading, suggesting that NO acts as better oxidizing agent than O2. The lowest determined ignition temperature with the presence of NO was found to be ca. 290°C for K–Fe3O4and ca. 240°C for K–Mn3O4. In the case of iron spinel based materials the changes of the observed work function upon K addition correlate withsoot oxidation reactivity, while for manganese spinel based materials such correlation is not observed. Whereas, for iron oxide catalyst the addition of potassium leads to the surface promotional effect, for manganese oxides potas- sium invokes more severe structural changes (formation of KMn4O8andKMn4O16).
Acknowledgments The project was financed by the Polish National Science Center awarded by decision number DEC-2011/01/B/ST4/ 00574
Open Access This article is distributed under the terms of the Creative Commons Attribution License which permits any use, dis- tribution, and reproduction in any medium, provided the original author(s) and the sourceare credited.
13