POLIMERY 2011, 56, nr6
461
MACIEJ CHOCZYÑSKI1)), BARBARA KRAJEWSKA1), ZDZIS£AW STÊGOWSKI2), JAROS£AW NÊCKI2)
Emission of styrene from polystyrene foam and of cyclopentane
from polyurethane foam — measurements and modelling
Summary — Due to toxicity of volatile organic compounds (VOC), assessment of their emission from polymer dry construction materials is of importance for the quality of the indoor environ- ment. Accordingly, in this work we studied emissions of styrene from polystyrene foam (PSf) and of cyclopentane from polyurethane foam (PURf). Both foams are common insulation materials. The partition (K) and diffusion (D) coefficients of these compounds in respective foams were deter- mined at temperature between 23—90 °C. The partition coefficients of foam-ambient gas system (KM-A) derived from the determined adsorption and desorption rate constants (kads, kdes) using the close-to-equilibrium theory and computer simulation, resulting in comparable values. The diffu- sion coefficients, by contrast, were obtained using three models based on sorption (DS), permea- tion (DP) and computer simulation (DC). In the first model, the foam is seen as a continuous phase, in the second model — as consisting of two phases where the VOC concentration is arithmetically averaged, while the third one assumes the inhomogeneous VOC distribution. Based on the same experimental data, three sets of diffusion coefficients were obtained (DS, DP, DC), disparate in va- lues, these disparities originating from the assumptions made in each model. The computer-simu- lation at relatively low migrant concentrations in the foam (styrene-PSf system), and the permea- tion model at high migrant concentrations (cyclopentane-PURf system) generated the diffusion coefficients comparable with results presented in the literature.
Keywords: styrene, cyclopentane, polystyrene foam, polyurethane foam, emission, computer
simulation.
EMISJA STYRENU Z PIANKI STYROPIANOWEJ I CYKLOPENTANU Z PIANKI POLIURETA- NOWEJ — POMIARY I MODELOWANIE
Streszczenie — Ze wzglêdu na toksycznoœæ lotnych zwi¹zków organicznych (volatile organic com- pounds — VOC), oznaczanie emisji tych zwi¹zków z polimerowych, suchych materia³ów budo- wlanych ma ogromne znaczenie z punktu widzenia jakoœci œrodowiska we wnêtrzu domów. W opisanej poni¿ej pracy zbadano kinetykê emisji styrenu z pianki styropianowej (PSf) oraz cyklo- pentanu z pianki poliuretanowej (PURf, rys. 1 i 2). Obydwie pianki s¹ powszechnie stosowanymi materia³ami izolacyjnymi. Oznaczono wspó³czynniki podzia³u (K) i dyfuzji (D) badanych zwi¹z- ków w piankach w zakresie temperatury 23—90 °C. Wspó³czynniki podzia³u w uk³adzie pian- ka–otaczaj¹cy gaz (KM-A) obliczono z wyznaczonych wartoœci sta³ych szybkoœci sorpcji i desorpcji (kads, kdes) zwi¹zków na piankach, z zastosowaniem kinetyki reakcji I rzêdu w pobli¿u stanu równo- wagi i symulacji komputerowej. Obydwie metody obliczeniowe da³y porównywalne wyniki (tabe- le 1—3). Natomiast do obliczenia wspó³czynników dyfuzji zwi¹zków w piankach, pos³u¿ono siê trzema modelami opartymi na: sorpcji zwi¹zków w piankach (DS), ich permeacji przez pianki (DP) b¹dŸ na symulacji komputerowej (DC). W modelu sorpcyjnym zak³ada siê, ¿e pianka jest faz¹ ci¹g³¹, podczas gdy w modelu permeacyjnym — sk³ada siê z dwóch faz, w których stê¿enie VOC jest uœrednione; model symulacyjny zak³ada niehomogeniczny rozk³ad stê¿enia VOC. Wychodz¹c z tego samego zestawu danych pomiarowych otrzymano trzy zestawy wspomnianych wspó³czynników dyfuzji (DP, DS, DC) ró¿ni¹cych siê wartoœciami (tabela 4). Ró¿nice te s¹ wyni- kiem za³o¿eñ poczynionych w ka¿dym modelu. Porównywalne z danymi literaturowymi (tabela
5) wartoœci wspó³czynników dyfuzji w obszarze wzglêdnie ma³ych stê¿eñ migranta w piance
1) Jagiellonian University, Faculty of Chemistry, 30-060 Kraków, Ingardena 3, Poland.
2) AGH-University of Science and Technology, Faculty of Physics and Applied Computer Science, 30-059 Kraków, Reymonta 19, Poland.
) Author for correspondence; e-mail: maciej.choczynski@uj.edu.pl

462
POLIMERY 2011, 56, nr6
(uk³ad styren-PSf) uzyskano metod¹ symulacji komputerowej, a w przypadku wiêkszych stê¿eñ (cyklopentan-PURf) — zgodnie z modelem permeacyjnym.
S³owa kluczowe: styren, cyklopentan, pianka styropianowa, pianka poliuretanowa, emisja, symu- lacja komputerowa.
Assessment of emissions of volatile organic com- pounds (VOC) from polymer dry materials used in con- struction industry is an important aspect of their phy- sico-chemical investigations [1—3], which is due to toxi- city of VOC. This may have impact on the quality of the indoor environment [4], on the health and general com- fort of the occupants in particular. VOC are introduced to the materials as additives to improve material properties or are present in the materials as residuals of polymeriza- tion processes [5]. An example of the first group of VOC is cyclopentane used as a blowing agent during polyure- thane foam manufacturing [6], and an example of the se- cond group is styrene, a monomer in the process of poly- styrene fabrication [7]. In addition to the toxicity analysis, VOC emissions are also studied to estimate the quality of polymeric materials and to investigate the ageing pro- cesses [8].
Emissions of VOC from polymeric materials are usu- ally determined by the American (ASTM D 5116-90) or European (ENV 13419) standard test methods. Typically, in these tests emissions are determined in a relatively short time (several days) using small chambers (volume lower than 1 m3) at ambient temperature (the measure- ments at temperatures >23 °C are infrequent [9]). How- ever, often the information on long term emission profiles in a full-scale chamber (indoor conditions) is necessary. Normally, such measurements are time-consuming and costly, and as a result, wherever possible, they are re- placed by the mathematical modeling of emissions [10—13].
The emission of VOC from polymeric materials is a process consisting of a diffusion through the material and a surface emission [2]. Diffusion, for a given system de- scribed by a diffusion coefficient, occurs under the con- centration gradient. Surface emission by contrast, con- sists of the partition on the material-air interface de- scribed by the partition coefficient, and further of the transport in the air (diffusion and convection) [2, 10]. The diffusion in the polymer and partition between the poly- mer surface and air are limiting phenomena in the emis- sion processes [10].
For a model of emission to be developed, the know- ledge of a number of input parameters is required. These include the initial concentrations of VOC in the material, in addition to partition and diffusion coefficients. The ini- tial concentration of VOC in the polymer material may be determined by various separation methods, for instance by dissolving a polymer sample followed by precipita- tion of the polymer [3], by headspace analysis [14, 15], complete evaporation of the sample to a gas phase [16], or extraction of the compound to an organic solvent.
The partition coefficients at material/gas interfaces defined as the ratio of VOC concentrations in the material phase to that in air at equilibrium conditions, are com- monly determined gravimetrically from the direct mea- surements of sorption on the material with use of the McBean balance [17, 18]. The measurements can also be performed indirectly with other techniques, such as inversed gas chromatography (IGC) [19—21], the men- tioned headspace technique (HS) [14, 22, 23], acoustic sensors (surface acoustic wave — SAW or thickness shear mode — TSM) [21, 24] and the vapor pressure method [25]. Alternatively, the partition coefficients may be ex- pressed as the ratio of VOC adsorption to desorption rate constants, and these are typically determined from the measurements of VOC sorption in dynamic experiments [26, 27].
The diffusion coefficients in the materials may be measured in two ways, namely by sorption and perme- ation [28]. Sorption methods, wherein sorption kinetics of the compound in the polymeric material is measured, make use of the relationship between the rates of sorption and of transport of the compound in the material repre- sented by the diffusion coefficient [29—32]. Under per- meation methods, the polymer material is used as a per- meable membrane and the amount of compound diffus- ing across the membrane at a constant concentration (pressure) gradient is measured, from which the diffu- sion coefficient is determined [33—35].
Foams are a special type of polymer materials. They are non-homogeneous (porous) materials that can be looked at as dual phase-materials consisting of gas (cells) and solid polymer (walls). Transport of VOC in a foam in- volves both diffusion in the gas phase and permeation through the cell walls [36]. These phenomena depend on the properties of the migrating compounds as well as on the structure of the foam (including its geometry, distri- bution of the cells, thickness of their walls) and polymer density. In describing mass transport through these mate- rials two approaches are commonly adopted. One as- sumes that the polymer material is homogeneous and that VOC are evenly distributed in the material [11, 37]. The other one by contrast, assumes that the material con- sists of two phases, where VOC are present as a gas in the cells and as an adsorbed phase in the polymer, but only those in the cells diffuse through the material [38, 39]. Typically, this approach requires the employment of a geometrical factor representing the structural properties of the foam [6, 36].
In this work we studied the emission (as VOC) of sty- rene from polystyrene foam and of cyclopentane from polyurethane foam. The rate constants of adsorption and

POLIMERY 2011, 56, nr6
463
desorption of styrene and of cyclopentane were deter- mined and used for the calculation of their material-air partition coefficients. Moreover, the rate constants were generated from a computer simulation, which was fur- ther utilized for the calculation of diffusion coefficients. In addition to the simulation, the diffusion coefficients were obtained using models based on sorption and per- meation. For the sorption we adopted the model that was used, as reported in the literature, for a packing mate- rial-food simulant system [13], while for the permeation we developed a model that takes into account the diffu- sion of the compound both dissolved in the polymer and present in the cells.
the compound in the cell wall, [c ], to that in the cell gas,
e
p
the following approach was used.
[ce ]. To calculate K
P-C
C
The experimentally derived initial concentration of the
compound, [c0 ], is the concentration in the whole mate-
M
rial. For a density-calculated solid polymer volume, the initial concentration of the compound in the polymer be- fore the partition process between the polymer and the
cell gas has occurred, [c0 ], can be expressed by:
p
[c0] = [c0 ] f
(4)
p	M P–M
where: fP-M — the ratio of the volume of the foam to that of the polymer.
The equilibrium concentration in the cell wall, [c ],
e
p
was calculated by subtracting the amounts of the com-
pound released to the cells, [c ], and to the chamber, [c ],
e
e
THEORY AND CALCULATION PROCEDURES
A
C
from the initial concentration [c0 ].
p
Furthermore, it was assumed that only those VOC molecules were released into ambient air, which had been transferred to the gas phase of the polymer. Two parallel processes of VOC distribution in the poly- mer-cell/gas-air system were assumed to take place. The first one is the partition of the compound between the polymer phase and cell gas consistent with the equi- librium condition:
Partition coefficients
The final mass transfer of VOC from the bulk of the material to the ambient phase at a given temperature is
determined by the partition coefficient with concentration, and defined as:
KM-A,
invariant
[ce ]
K M- A  M
(1)
[ce ]
0
A
[cP ]
e
[c ] 
(5)
C
where: [ce ] and [c ] — the equilibrium VOC concentrations
e
(K	 f
)
P-C	P-M
A
M
in a material and ambient phase, respectively.
For low concentrations the linear Henry’s sorption applies [40, 41].
Alternatively, the partition coefficient KM-A may be ex- pressed as the ratio of the adsorption kads and desorption kdes rate constants:
The process provided the molecules to the cells of the foam.
The second process, on the other hand, resulted in both the reduction of the concentration of the compound in the cell gas and its growth in the external phase. Fi- nally, the internal partition coefficient KP-C is expressed by the following equation:
 kads
K
(2)
M-A
k
des
f	[c 0 ]
[c 0 ] PM P	[ce ] f
To determine the partition coefficients
K	from
f
A M  A PM
P
[ce ]
M-A
(K	 f	)
 P PC	PM
equation (2), we derived the rate constants kads and kdes
(6)
K PC
[ce ]
f M  A [c 0 ]
from the experimental data with use of the close-to-equi- librium kinetics [42]:
C
P
e
[c A ] f M  A
(K PC  f PM )
The f factors were calculated from the foam and poly- mer densities and from the geometry of the emission
d[cA ]  k
f	)  k	[c0 ]
[c ]  k	[c
]  [c ](k	 k
A	ads	des M  A	des M
ads A	des
M
d t
chamber. To calculate the partition coefficient K	, equa-
(3)
P-C
tion (6) was transformed into the second degree polyno- mial function and KP-C was taken as its non-zero, positive solution. Clearly, the partition coefficient between the
where: fM-A — the ratio of the volume of the ambient phase to that of the foam, [cA] and [cM] — the concentrations of the com-
pound in the ambient gas and in the foam, respectively, [c0 ] —
foamed polymer and the external gas phase K
[equa-
M-A
M
tion (2)] does not have the same value as the partition co-
the initial concentration of the compound in the foam.
The rate constants were determined from the inter-
efficient between the polymer and the cell gas KP-C [equa- tion (6)], which is due to the structural and geometrical factors.
cepts and slopes of the linear dependencies of the process
rates on [cA] according to equation (3). Additionally, we developed three-dimensional computer simulations to generate the adsorption/desorption rate constants and the diffusion coefficients by the best fitting to the experi- mental data (see further text).
In contrast to KM-A, the internal partition coefficient KP-C describes the distribution of the compound between the polymer and the cell gas, and accordingly is ex- pressed by the ratio of the equilibrium concentration of
Diffusion coefficients
The starting point to describe the transfer of VOC both in the material and in the inner gas phase is Fick’s second law:
2
d[cM ] 	d [cM ]
(7)
D
d l 2
d t

464
POLIMERY 2011, 56, nr6
where: [cM] — the concentration of the compound in the mate- rial, D — its diffusion coefficient in the material, t — time, l — the position (length).
The independence of diffusion coefficient from the position, time and concentration is a basic assumption in the emission models. The concentrations of VOC are usu- ally low, which is why it can be assumed that swelling effects do not affect the diffusivity.
To derive the diffusion coefficients, models of mass transfer of VOC within polymer materials are used. In this work the following three models were employed: sorption, permeation and computational. From them three diffusion coefficients for each studied system were obtained, accordingly DS, DP and DC. The sorption and computational models assume that the initial distribu- tion of the diffusing compound in the foam is homo- geneous. However, in the sorption model the concentra- tion distributions are constant during a single measure- ment, while in the computational model the diffusion in the three dimensional space implicates a step-by-step growth of heterogeneity of concentration distribution, and a resulting effect on the concentration gradient.
A feature of the permeation model, on the other hand, is
that it distinguishes two phases inside the foam, namely polymer and gas, between which the concentration dis- tribution is determined by the internal partition coeffi- cient KP-C.
from the cell gas through the cell wall. The model divides the migrating compound into two populations. One po- pulation is dissolved in the polymer, while the other one is present in the cell gas, both in the amounts governed by
the internal partition coefficient
KP-C,
calculated from
equation (6). Further, the first population diffuses only in the solid polymer, hence covers a distance that encom-
passes only a solid part of the foam, while the second population migrates from cell to cell across the solid polymer, hence covers a distance equal to the length of the foam. Both the above distances were averaged to ob- tain the weighted means of the migration paths in the three dimensional space. In reality, due to the fact that the fraction of gas phases in foams is high, a majority of mi- grant molecules in foams proceed by doing multiple per- meations through the polymer phase. The diffusion in the gas phase is a number of orders of magnitude faster than in the polymer phase, which is why the resulting dif- fusion coefficients have the values between those charac- teristic of the two phases. In this model the multiple ad- sorption and desorption processes are seen as a single act expressed by the partition coefficient, and the whole polymer phase is treated as homogeneous.
Diffusion coefficients were calculated from equation
(7) where the concentration gradients were defined as a sum of the spatially averaged gradients: one on a poly- mer-cells distance (only polymer fraction thickness) and the other one — on a cell-ambient phase distance (mate- rial thickness). The permeation model includes the con- centrations both in the external gas phase, cA, and in the cell gas, cC, the latter calculated from the formula:
Sorption model
The sorption model adopted here was previously de- veloped to describe VOC transport from polymer pack- ing materials to food simulants [7, 13]. In the model a sample is represented by a flat sheet, infinite in thickness. This ensures that the interior concentration is not influ- enced by the processes. When the external (fluid) phase is well mixed, the compounds released by the material are uniformly distributed in the fluid phase. If the volume of the fluid is assumed to be infinite, the concentrations of the compounds in this phase are negligibly low. In such a case the amount of the desorbed compound is expressed
[c0 ]
P
cC  
(9)

KPC  f PM
It was assumed that the distance covered by the diffu- sion, l, was equal to half the sample thickness. In the ex- periment, the rate of the migrant concentration cM change in the material was directly proportional to the concen- tration cA change in the chromatographically analyzed external phase, with fM-A equal to the ratio of the volume of the external phase to that of the material, being a factor. It was assumed that the equilibrium in the cell-polymer systems was reached rapidly. Clearly, the permeation model proposed is a simplification of the real diffusion in the foam in that it ignores the fact that the mass transfer consists primarily of the cell to cell migration.
by:
Dt 
M  2[c0 ]

(8)
t	M
ð
where: Mt — the amount of the compound released by a unit of polymer area at time t.
The mechanical fan operating in the chamber ensured that the external phase, substantially greater than the ma- terial volume, was homogeneous. Importantly, equation
(8) ignores the partition because of the relatively low con- centrations of the compounds in the external phase.
Computer simulation
The computational model of the VOC transport in the foam was developed under three theoretical as- sumptions: a) the motion of the compound inside the foam is described by the diffusion [equation (7)], b) the compound exchange between the foam surface and the ambient air consists of adsorption and desorption pro- cesses described by equation (2), c) the transport of the compound in the air surrounding the foam is several
Permeation model
In this approach the migration of a VOC from the foam to the external phase consists of the diffusion in the solid phase of the foam (polymer) and the permeation

POLIMERY 2011, 56, nr6
465
orders of magnitude faster than inside the foam. In consequence, in the model the three-dimensional con- centration of the compound in the ambient air is uni- form and is exclusively a function of time. A difference between the permeation and the computational model lies in the approach to the structure of the investigated material, namely the computational model does not take into account the existence of the gas and solid phases.
The computational modeling was created using the fi- nite elements method. The mesh grid for the foam sam- ples had 126 000 (30 × 30 × 140) cubic cells. The boundary and the initial conditions were the same as in the experi- ments. The initial styrene and cyclopentane concentra- tions in the ambient air were set to null and the initial con- centrations in the foams were assumed to be homo- geneous.
The first order differential method was used for solv- ing equation (3) and (7) for the process simulation. Dur- ing the simulation the time step interval of one second
Apparatus and experimental procedures
The emissions of styrene and cyclopentane from the respective foams were measured in a test chamber, 800 cm3 in volume. The chamber, placed in a gas thermostat, was equipped with a temperature sensor and a fan, the latter to ensure effective mixing of a gas in the chamber interior. The foam samples were set on a perforated stain- less steel support and rapidly introduced into the cham- ber, after which the chamber was tightly closed. The gas in the chamber was analyzed for styrene or cyclopentane at time intervals on a gas chromatograph. For that the chamber was directly connected to a HP 6890 gas chromatograph equipped with a HP-5MS column (5 % diphenyl + 95 % polydimethylsiloxane, 30 m long,
0.25 mm internal diameter, film thickness 0.25 µm). HP 5973 mass quadruple spectrometer was used as the detec- tor, working in SIM mode (Single Ion Monitoring) at 104 m/z (mass to charge ratio) for styrene, and at 42 m/z for cyclopentane. HP 7694E headspace autosampler was slightly modified to cooperate with the sample loop injec- tor of the gas chromatograph. Gas flow, forced by the membrane pump, was directed from the chamber through the sample loop to return to the chamber. When the six-port valve altered its position, the carrier gas washed out the compounds from the sample loop to the chromatograph inlet. The time required to develop a chromatogram and to prepare the chromatograph for a subsequent analysis (7—10 min) was a limiting factor for the time intervals applied. The emission measurement se- ries were carried out for both kinds of the foams (PSf and PURf) at the following chamber temperatures: 23, 30, 40, 50, 60, 70, 80 and 90 °C, with an accuracy of ±0.5 °C.
The calibration of the system for the styrene and cyclo- pentane determinations was carried out according to the exponential dilution procedure [44]. The gas standards were prepared in helium. The procedure allowed collect- ing numerous calibration points within the linear range 0.0001—1 µg cm-3 for styrene and 5—10 000 µg cm-3 for cyclopentane.
To determine the initial concentration of styrene in- side PSf, a sample of the foam of about 10 cm3 in volume was dissolved in 2 cm3 of dichloromethane and then the polymer was precipitated with 1 cm3 of methanol [3]. The concentration of styrene in the methanol-dichloro- methane mixture was carried out using the external cali- bration done in the same mixture of the solvents. The re- sulting concentration of styrene in PSf was determined to be 5.01 ± 0.20 µg cm-3 of PSf.
Unlike polystyrene, polyurethane foams are insoluble in most organic solvents, which is why the initial concen- tration of cyclopentane in PURf was determined sepa- rately in the cell gas and in the solid polymer. To analyze the cell gas, a PURf sample was crushed in a hermetic stainless steel container at 100 °C and the released gas was analyzed by GC according to the procedure reported in the literature [36], only slightly modified. To determine
was applied. The coefficients D,
and
were the
kads
kdes
parameters of the model. The spatial and temporal func-
tion of the concentrations of the compounds in the poly- mers, cP, and the time function of their concentrations in the air, cA, were obtained from the simulations. The va- lues of D, kads and kdes were derived based on the experi- mental and simulated sets of data. To this end the simula- tion code was combined with the optimization code. The optimization code used the Nelder-Mead Simplex Method [43] to find the optimal values of the constants of interest by comparing the experimental and simulated data. The iteration method was applied and the least squares method was used for optimization. Both codes were prepared in Matlab computation environment. Using a fast PC one set of data was computed within 2—4 hours.
EXPERIMENTAL
Materials
Polystyrene (PSf) and polyurethane (PURf) foams were commercial products. PSf (density 0.025 g cm-3) was in the form of a board and PURf (density
0.037 g cm-3) was a rigid heating pipe insulation. The samples to be analyzed were cut out of the interior of the bigger foam pieces. For the density measurements the samples 15 × 10 × 8 cm were weighed with ±1 mg accuracy, giving the uncertainty of density determina- tions <0.01 %. For an emission experiment four sam- ples with the total volume of 30 cm3 and the total sur- face area of 120 cm2 were used. High purity helium with 2 ppm oxygen content, containing less then 3 ppm of moisture, was used as the carrier gas. Styrene and cyclopentane (both 99.8 %) were supplied by Fluka, methanol and dichloromethane (both of HPLC grade) supplied by Merck.

466
POLIMERY 2011, 56, nr6
b)
a)
20
18
16
14
12
10
8
6
4
2
18
16
14
12
10
8
6
4
2
0
0
0
0
20
100
120
40
60
80
100
120
140
20
40
60
80
140
Time, min
Time, min
Fig. 1. Kinetic curves of the emission of: (a) styrene from polystyrene foam, and (b) cyclopentane from polyurethane foam, at 30 °C
♦, 50 °C ◊, 60 °C .._ , 70 °C ,6., 80 °C e, 90 °C O
the cyclopentane concentration in the solid polyurethane, the crushed PURf was frozen and ground into powder. Then it was placed in the hermetic glass container and the cyclopentane concentration was determined by static headspace technique at 280 °C. The overall concentration of cyclopentane in PURf was taken as the sum of that in the cell gas and in the polymer and it turned at to be 475 ± 25 µg cm-3 of PURf. The calibration curves for the cyclo- pentane determination were obtained with the use of the hermetic stainless steel and glass containers.
achieved was around 100 min for both styrene-PSf and cyclopentane-PURf systems. The amount of the com- pounds released from the foams increased strongly with temperature. For both systems these curves were best de- scribed by hyperboles. From the equations of the hyper- boles, the process rates dcA/dt at different times of the process were calculated.
Adsorption and desorption rate constants
To calculate the adsorption and desorption rate con- stants, kads and kdes, the process rates dcA/dt were plotted against cA according to equation (3). The concentrations of the compounds in the materials and in the cell and polymer phases were calculated from the mass balance using the initial concentrations of the compounds in the foams, the concentrations in the chamber, as well as the volumes of the chamber, of the foams and of the solid polymers in the foams.
The plots for different temperatures are presented in Fig. 2a for styrene-PSf and in Fig. 2b for cyclopen- tane-PURf. In accordance with equation (3) the rate con-
RESULTS AND DISCUSSION
Emission measurements
The concentrations of styrene and of cyclopentane released from the foams to the gaseous phase were expressed as chromatographic peak areas. The typical kinetic curves describing the emissions for different tem- peratures are presented in Fig. 1a for styrene-PSf and Fig. 1b for cyclopentane-PURf. The observed time for the equilibrium between the foams and the ambient gas to be
a)
b)
0.60
0.016
0.014
0.012
0.010
0.008
0.006
0.004
0.002
0.000
0.50
0.40
0.30
0.20
0.10
0.00
0.000
0.001
0.002
0.003
0.004
0.005
0.00	0.02	0.04	0.06	0.08	0.10	0.12	0.14
-3
-3
Gas phase concentration, g·cm
Gas phase concentration, mg·cm
Fig. 2. Process rate as a function of concentration in the chamber for the emission of: (a) styrene from polystyrene foam, and (b) cyc-
lopentane from polyurethane foam, at 23 °C ♦, 40 °C ◊, 50 °C ,6., 60 °C e, 70 °C O, 80 °C ■, 90 °C □
2	-3	-1
Process rate·10 , g·cm ·min
-4
Intensity·10 , a.u.
2
-3
-1
Process rate·10 , mg·cm ·min
-5
Intensity·10 , a.u.

POLIMERY 2011, 56, nr6
467
stants of desorption kdes and of adsorption kads were calcu- lated from the values of intercepts and slopes of the lines. The results are listed in Table 1. The computer simula- tion-derived rate constants kads and kdes by contrast, are presented in Table 2.
remaining in a foam rather than in gas phase. Second, the adsorption rate constants kads decreased slowly with an increase in temperature within the studied range of 23—90 °C, only two- to three-fold on average. Third, un-
like the rate constants of adsorption	the rate con-
kads,
stants of desorption	increased sharply with an in-
kdes
crease in temperature, one to two orders of magnitude within the same temperature range.
T a b l e 1. Rate constants of adsorption and desorption, kads and kdes, and partition coefficients KM-A for styrene-PSf and cyclopen- tane-PURf systems for different temperatures derived from the close-to- equilibrium theory
Partition coefficients
Table 1 and 2 also present the partition coefficients, KM-A, of styrene and of cyclopentane between the respec- tive polymer foams and gas phase, calculated from equa- tion (2) according to the applied methods: close-to-equili- brium theory and computer simulation. In keeping with
the above described trends in k
and k
variations, the
des
ads
KM-A coefficients obtained by both these methods are simi-
lar in value for each system. The partition coefficients of cyclopentane, however, are significantly higher than those of styrene, due to good sorption properties of polyurethane for VOC. The KM-A values obtained for styrene-PSf gene- rally comply with the values reported in the literature, e.g. 260 at 25 °C [29], but for cyclopentane-PURf, they are sig- nificantly different, e.g. 6 at 21 °C [45].
From the adsorption and desorption rate constants obtained at different temperatures, the activation ener- gies Ea of adsorption and desorption were calculated using the Arrhenius equation:
Ea
T a b l e 2. Rate constants of adsorption and desorption, kads and kdes, and partition coefficients KM-A for styrene-PSf and cyclopen- tane-PURf systems for different temperatures derived from the computational model
k  Ae
RT
The results are also compiled in Table 1 and 2. For ad-
sorption, E appeared to have a negative value both for
a
styrene and cyclopentane, thereby indicating the ten- dency of the compounds to remain in the foams. Gene- rally, processes exhibiting negative activation energies are typically barrierless. Indeed, the activation energies of organic adsorption on polymers are known to be low, often close to zero [46]. This is why the heat of adsorption may be viewed as corresponding to the activation ener- gies of desorption, shown here to have relatively high positive values. For instance, in a study of hydrocarbon desorption (C6—C14) on low density polyethylene, enthalpies of desorption between 33.7 kJ mol-1 (2,4-di- methylheptane) and 87.1 kJ mol-1 (alkene C11) were re- corded [47]. In another study, the measurements of sty- rene sorption on polystyrene by inversed gas chromato- graphy (IGC) technique at temperatures between 70 and 120 °C produced the heat of sorption equal to 42 and 71 kJ mol-1 below and above glass transition (~95 °C), respec- tively [19]. In conclusion, it can be stated that both models applied generated consistent values of the activation energy of desorption that are in agreement with the literature data.
In addition to the partition coefficients KM-A of styrene and cyclopentane between the respective foams and the ambient air, also their internal partition coefficients KP-C
As shown in Table 1 and 2, the values of kads and kdes obtained from equation (3) are on average one order of magnitude lower than those obtained from the computer simulations at the same temperatures, the difference be- tween them increasing with an increase in temperature. However, their regular variations with temperature be- tween 23 and 90 °C within each set of results revealed cer- tain characteristic behaviors of the analysed systems. First, as expected, the adsorption exceeded the desorp- tion in both styrene-PSf and cyclopentane-PURf systems, the rate constants of desorption being one to four orders of magnitude lower than those of adsorption at the same temperatures. This implies that the compounds favor

Styrene-PSf
Cyclopentane-PURf
T, °C
kads, s-1
kdes, s-1
KM-A
kads, s-1
kdes, s-1
KM-A
23
30
40
50
60
70
80
90
Ea, kJ·mol-1
2.6 · 10-3
2.7 · 10-3
2.8 · 10-3
2.9 · 10-3
3.0 · 10-3
2.9 · 10-3
2.7 · 10-3
1.8 · 10-3
-2±2
6.3 · 10-6
1.0 · 10-5
1.5 · 10-5
2.2 · 10-5
3.9 · 10-5
6.9 · 10-5
1.0 · 10-4
1.9 · 10-4
43±2
417
268
190
131
76
42
26
10

4.1 · 10-3
3.9 · 10-3
3.7 · 10-3
3.5 · 10-3
2.9 · 10-3
2.1 · 10-3
2.1 · 10-3
1.9 · 10-3
-11±1
5.3 · 10-7
1.1 · 10-6
2.2 · 10-6
3.7 · 10-6
5.3 · 10-6
1.1 · 10-5
2.4 · 10-5
4.7 · 10-5
57±2
7789
3637
1727
946
552
184
88
40

Styrene-PSf
Cyclopentane-PURf
T, °C
kads, s-1
kdes, s-1
KM-A
kads, s-1
kdes, s-1
KM-A
23
30
40
50
60
70
80
90
Ea, kJ·mol-1
5.9 · 10-4
5.8 · 10-4
5.8 · 10-4
5.7 · 10-4
5.5 · 10-4
4.7 · 10-4
3.9 · 10-4
1.9 · 10-4
-11±4
1.4 · 10-6
2.1 · 10-6
3.0 · 10-6
4.3 · 10-6
7.2 · 10-6
1.1 · 10-5
1.6 · 10-5
2.6 · 10-5
38±1
429
277
196
133
76
41
24
7

1.1 · 10-3
9.6 · 10-4
7.9 · 10-4
7.4 · 10-4
6.5 · 10-4
5.5 · 10-4
4.8 · 10-4
3.8 · 10-4
-13±1
1.3 · 10-7
2.5 · 10-7
4.0 · 10-7
6.6 · 10-7
9.6 · 10-7
2.1 · 10-6
3.7 · 10-6
6.8 · 10-6
50±2
8256
3901
1956
1126
684
264
130
56

468
POLIMERY 2011, 56, nr6
corresponding to the polymer-cell systems, were ob- tained from the experimental data. The coefficients were computed using equation (6) and their values are pre- sented in Table 3. Their values were found to be higher than those reported in the literature for bulk polymers (systems polymer-air) and composites. The typical values of such partition coefficients commonly fall in the range from several thousands at room temperature to a few hundreds at 80 °C [24, 48], depending on the chemical affinity and VOC molecular weight. For instance, for sty- rene on solid polystyrene, the partition coefficients amount to 67—6.5 in the temperature range from 70 to 110 °C [19]. When extrapolated to 20 °C, the above data give the partition coefficient equal to 10 500, i.e. some three times lower than the internal partition coefficient obtained in this study. Unlike for polystyrene, there are no direct literature reports on partition of homogeneous solid polyurethane. For polyurethane foam, however, the values of cyclopentane partition coefficients calculated from the solubility coefficients for the polyurethane phase extracted from the foam [36], amount to 100 000— 280 000 at 23—25 °C.
perimental parameters rather than coefficients describ- ing the true VOC polymer/external phase partition. This notwithstanding, the coefficients constitute an effort to acquire effective and practical parameters that could be used in further calculations of diffusion coefficients.
Diffusion coefficients
The diffusion coefficients of styrene in PSf and of cyc- lopentane in PURf were obtained from the three pro- posed models — sorption, permeation and computer simulation; accordingly they were designated as DS, DP and DC. The coefficients DP and DS were calculated from equation (7) and (8), respectively, wherein the data needed for calculations, i.e. the concentration of the com- pounds in the foams and the mass of the compounds desorbed from the foams, were read out from the emis- sion kinetic curves (Fig. 1). Due to discrete character of concentration data, DP was calculated using differential form of equation (7) by summation over the time before the equilibrium was estabilished. The coefficient DC, by contrast, was a parameter in the computational simula- tions used together with the adsorption and desorption rate constants to describe the observed courses of emissions. The results are presented in Table 4.
The values of D differ from each other by one to four
orders of magnitude, depending on the system and tem- perature. The computer-simulation derived values DC are always lower than those experimentally derived using sorption DS and permeation DP models, whereas the DS values are always higher (styrene-PSf) or rather lower (cyclopentane-PURf) than the DP values. Appa- rently, these disparities seen in the diffusion coefficients originate from the assumptions made in each model ap- plied showing how big an impact the data analysis cho- sen has on the final values [49]. For comparison purposes, Table 5 gives a selection of diffusion coefficients reported in the literature for the same VOC-foam systems, how- ever for the foams of higher densities. In case of the sty- rene-PSf system, the computer simulation generated re- sults most comparable to diffusion coefficients quoted in
T a b l e 3. Internal partition coefficients KP-C for styrene in PSf and of cyclopentane in PURf
Owing to the complex geometrical structure of both polymers and cell phases in the foams, in our opinion in- ternal partition coefficients KP-C should be treated as ex-
T a b l e 4. Diffusion coefficients [calculated from the permeation (DP), sorption (DS) and computer simulation (DC) models] of styrene in PSf and of cyclopentane in PURf

Styrene-PSf (density 0.025 g cm-3)
Cyclopentane-PURf (density 0.037 g cm-3)
T, °C
DP, cm2 s-1
DS, cm2 s-1
DC, cm2 s-1
DP, cm2 s-1
DS, cm2 s-1
DC, cm2 s-1
23
30
40
50
60
70
80
90
Ea, kJ mol-1
1.6 · 10-9
2.3 · 10-9
3.2 · 10-9
4.5 · 10-9
6.9 · 10-9
1.1 · 10-8
1.4 · 10-8
2.1 · 10-8
33±1
1.7 · 10-8
3.8 · 10-8
7.2 · 10-8
1.4 · 10-7
3.3 · 10-7
7.7 · 10-7
1.4 · 10-6
3.0 · 10-6
68±2
8.6 · 10-11
1.6 · 10-10
2.8 · 10-10
4.7 · 10-10
7.8 · 10-10
1.3 · 10-9
1.9 · 10-9
2.9 · 10-9
48±2
7.5 · 10-10
1.5 · 10-9
3.0 · 10-9
5.2 · 10-9
8.4 · 10-8
2.0 · 10-8
3.8 · 10-8
7.1 · 10-8
59±2
8.2 · 10-11
4.0 · 10-10
1.5 · 10-9
4.5 · 10-9
1.2 · 10-8
6.7 · 10-8
2.2 · 10-7
7.9 · 10-7
117±4
3.3 · 10-14
2.0 · 10-13
1.1 · 10-12
5.1 · 10-12
2.2 · 10-11
9.6 · 10-11
3.0 · 10-10
1.2 · 10-9
137±3
T, °C
Styrene-PSf
Cyclopentane-PURf
23
30
40
50
60
70
80
90
32 243
21 426
15 690
11 279
7274
4793
3600
2427
214 475
102 023
51 412
29 908
18 504
7622
4144
2184

POLIMERY 2011, 56, nr6
469
the literature. Permeation assumption delivered good consistence of D data for cyclopentane-PURf system.
methods, namely the close-to-equilibrium approach and a computer simulation, where the rate constants together with the effective diffusion coefficients were iterative pa- rameters relating the experimental data with the simula- tion of the concentration distribution inside the foams. The kads and kdes values for both styrene and cyclopentane obtained by the simulation were found higher than by the close-to-equilibrium approach, but the partition coeffi- cients determined by both methods were comparable. Unlike the partition coefficients, the adsorption/desorp- tion rate constants for the studied systems are not avail- able in the literature.
On the basis of the sorption, permeation and compu- tational models, three different sets of diffusion coeffi- cients were obtained for each studied system within the chosen temperature range. The computer-simulation de- rived diffusion coefficients were found to be comparable with the literature data for the system that consisted of relative low migrant concentrations in the foam (sty- rene-PSf), while for the system where migrant concentra- tions in the foam were significantly higher (cyclopen- tane-PURf) — permeation model was applied. The diffe- rent D coefficients varying among the models generated different values of the activation energy; good agreement between the experimental results and literature data was observed for DP in cyclopentane-PURf system.
REFERENCES
T a b l e 5. Diffusion coefficients of styrene in PSf (density
0.042—0.114 g·cm-3) [3] and of cyclopentane in PURf (density 0.061—0.071 g·cm-3) [50] reported in the literature
) Data taken from ref. [29].
) 23—60 °C.
In all the cases studied the diffusion coefficients in- creased with temperature, resulting in positive activation energies of diffusion (Table 4). Values of energies were found to be two times higher for DS in comparison to DP. The magnitudes of the energies, like the diffusion coeffi- cients, depended on the model applied. Their magni- tudes are comparable with those reported in the litera- ture (Table 5).
1.
2.
3.
Yu C., Crump D.: Build. Environ. 1998, 33, 57. Haghighat F., de Bellis L.: Build. Environ. 1998, 33, 261.
Lickly T. D., Lehr K. M., Welsh G. C.: Food Chem. Toxicol.
1995, 33, 475.
Wolkoff P.: Indoor Air Suppl. 1995, 3, 9.
Wolkoff P.: Sci. Total Environ. 1999, 227, 197.
Bart G. C. J., Du Cauze De Nazelle G. M. R.: J. Cell. Plast.
1993, 29, 29.
Crump D., Squire R. W., Yu C. W. F.: Indoor and Built Environ.
1997, 6, 45.
Singh S. N., Nitru M., Dedecker K.: J. Cell. Plast. 2003, 39, 265.
Wolkoff P.: Atmos. Environ. 1998, 329, 2659.
4.
5.
6.
CONCLUSIONS
This work presents results of experiments aiming at quantification of emissions of styrene from polystyrene foam (PSf) and of cyclopentane from polyurethane foam (PURf). Two approaches were applied to determine the adsorption and desorption rate constants of the VOC, and three models, based on sorption, permeation and computer simulation, to determine the diffusion coeffi- cients. A gas chromatograph-coupled measurement chamber was applied — which enabled the elimination of the pre-concentration procedures of the analyzed gases. The mass detector proved to give satisfactory detection limits as well as linearity over wide VOC concentration ranges and expected precision. The emission measure- ments were done in static conditions, at temperatures within the range of 23—90 °C.
The release of the VOC from the foams expressed by a chromatographic peak area over time was best described by a hyperbolic function. The partition coefficients of the VOC between the respective foams and air were deter- mined as the ratio of the rate constants of adsorption to desorption. The rate constants were obtained using two
7.
8.
9.
1. Huang H., Haghighat F.: Build. Environ. 2002, 37, 1349.
2. Haghighat F., Huang H.: Build. Environ. 2003, 38, 1007.
3. Lickly T. D., Breder C. V., Rainey M. L.: Regul. Toxicol. Pharm.
1995, 21, 406.
1. Reid R. C., Sidman K. R., Schwope A. D., Till D. E.: Ind. Eng. Chem. Prod. Res. Dev. 1980, 19, 580.
2. Trzeszczyñski J., Huzar E.: Chromatographia 2001, 53, 534.
3. Wenzl T., Lankmayr E. P.: Anal. Bioanal. Chem. 2002, 372, 649.
4. Chai X.-S., Hou Q. X., Schork F. J.: J. Chromatogr. 2004, A1040, 163.
5. Cox S. S., Zhao D., Little J. C.: Atmos. Environ. 2001, 35, 3823.
6. Zhao D., Little J. C., Cox S. S.: J. Environ. Eng. 2004, 130, 983.
7. Miltz J., Rosen-Doddy V.: Eur. Polym. J. 1986, 22, 327.
8. Kontominas M. G., Gavara R., Giacin J. R.: Eur. Polym. J.
1994, 30, 265.

Styrene-PSf
Cyclopentane-PURf
T, °C
DS, cm2 s-1
DP, cm2 s-1
4.5
21
23
25
40
49
60
66
90
Ea, kJ mol-1
8.8 · 10-12
(1.0—8.8) · 10-11
—
6.2 · 10-8)
— (2.7—9.5) · 10-10
— (2.5—4.8) · 10-9

79—100
—
—
6· 10-10
—
4· 10-9
—
7· 10-9
—
1· 10-8
60)

470
POLIMERY 2011, 56, nr6
1. Grate J. W., Klusty M., McGill R. A., Abraham M. H., Whit- ing G., Andonian-Haftvan J.: Anal. Chem. 1992, 64, 610.
2. Martos P. A., Pawliszyn J.: Anal. Chem. 1997, 69, 206.
3. De Coensel N., Desmet K., Górecki T., Sandra P.: J. Chromatogr. 2007, A1150, 183.
4. Grate J. W., Kaganove S. N., Bhethanabotla V. R.: Anal. Chem.
1998, 70, 199.
1. Bawn C. E. H., Patel R. D.: Trans. Faraday Soc. 1956, 52, 1664.
2. Jørgensen R. B., Bjørseth O., Malvik B.: Indoor Air 1999, 9, 2.
3. Jørgensen R. B., Dokka T. H., Bjørseth O.: Indoor Air 2000, 10, 27.
4. Crank J.: In “Diffusion in Polymers” (Eds. Crank J., Park G. S.), Academic Press Inc., London, New York 1968, pp. 1—39.
5. Yuan H., Little J. C., Hodgson A. T.: Atmos. Environ. 2007, 41, 3241.
6. Perez-Blanco M., Hammons R. J., Danner R. P.: J. Appl. Polym. Sci. 2010, 116, 2359.
7. Vopièka O., Hynek V., Friess K., Šipek M., Sysel P.: Chem. Listy 2009, 103, 310.
8. Choi O. K., Jitsunari F., Asakawa F., Lee D. S.: Food Addit. Contam. 2005, 22, 693.
9. Fialová K., Petrychkovych R., Sharma M., Uchytil P.: J. Membr. Sci. 2006, 275, 166.
10. Uchytil P., Petrièkoviè R.: J. Membr. Sci. 2002, 209, 67.
11. Maddinelli G., Iwanski P., Callaioli A., Ravanetti G. P.: Int. J. Polym. Anal. Ch. 2006, 11, 147.
1. Mangs S.: “Insulation Materials in District Heating Pipes”, PhD thesis, Chalmers University of Technology, Göteborg, Sweden 2005.
2. Yang X., Chen Q., Zhang J. S., Magee R., Zeng J., Shaw C. Y.:
Build. Environ. 2001, 36, 1099.
1. Meininghaus R., Gunnarsen L., Knudsen H. N.: Environ. Sci. Technol. 2000, 34, 3101.
2. Murakami S., Kato S., Ito K., Zhu Q.: Indoor Air 2003, 13
Suppl 6, 20.
1. Klopffer M. H., Flaconneche B.: Oil Gas Sci. Technol. 2001, 56, 223.
2. Soney C. G., Sabu T.: Prog. Polym. Sci. 2001, 26, 985.
3. Atkins P. W.: “Physical Chemistry”, PWN, Warszawa 2001, pp. 735—763.
4. Lagarias J. C., Reeds J. A., Wright M. H., Wright P. E.: SIAM J. Optimiz. 1998, 9, 112.
5. Ritter J. J., Adams N. K.: Anal. Chem. 1976, 48, 612.
6. Kamprad I., Goss K.-U.: Anal. Chem. 2007, 79, 4222.
7. ten Hulscher Th. E. M., Cornelissen G.: Chemosphere 1996, 32, 609.
8. Hodgson S. C., O’Connor M. J., Casey R. J., Bigger S. W.: J. Agric. Food Chem. 1998, 46, 1397.
9. Sabzi F., Boushehri A.: Eur. Polym. J. 2005, 41, 2067.
10. Haghighat F., Lee C.-S., Ghaly W. S.: Indoor Air 2002, 12, 81.
11. Olson M. E., Ulf J., Fröling M., Mangs S., Ramnäs O.: J. Cell. Plast. 2002, 38, 177.
Received 24 VI 2010.