MicrochimActa(2015)182:119–127DOI10.1007/s00604-014-1307-5
Rhodamine6Gconjugatedtogoldnanoparticlesaslabelsforboth SERS andfluorescencestudies on live endothelialcells
Aleksandra Jaworska&TomaszWojcik&Kamilla Malek&Urszula Kwolek&Mariusz Kepczynski&Abu A. Ansary&Stefan Chlopicki&Malgorzata Baranska
Received: 14 April 2014 / Accepted: 28 May 2014 / Published online: 19 June 2014
#TheAuthor(s)2014.ThisarticleispublishedwithopenaccessatSpringerlink.com
AbstractFluorescenceandsurface-enhancedRamanscatter- ing (SERS) spectroscopy were employed to investigate the cellular uptake of rhodamine 6G (R6G) alone and of R6Gloadedwithgoldnanoparticles(AuNPs)byendothelial cells.R6GplaystheroleofaRamanreporterinSERSbutalso displays strong fluorescence. The presence of bare R6G molecules and R6G-AuNPs in the cytoplasm of the cells is detectedviathe2Dfluorescenceofthedyeaftera0.5hofthe incubationwithR6GandR6G-AuNPs,andthentheconcen- tration of the dye increases within 4 h of exposure. The examination of the cellular uptake of the R6G and R6G- AuNPs species at different temperatures suggests that the internalization of the R6G-AuNPs into endothelial cells oc- cursmainlyviaendocytosis.3DfluorescenceimagingofR6G insidecellsrevealsinhomogeneousdistributionofthedyein thecytoplasm.TheSERSsignaloftheRamanreporterinside the cell disappears after 2 h of incubation withR6G-AuNPs and then amino acid residues, purines and pyrimidines be- come SERS-active via their interactions with the gold. The resultshighlightthesignificanceofusingmultipletechniques
to cover a spectrum of issues in the application of SERS nanosensors for probing an intracellular environment under comparable and standardized conditions.
KeywordsEndothelium.SERSimaging.2Dand3D fluorescence.Rhodamine6G.Cellularuptake
Introduction
Raman spectroscopy is a method that enables vibrational modes of individual bonds to be probed optically and has been widely employed in various biomedical experiments [1,2].WhiletheRamanscatteringisaweakeffectchallenging tomeasurespectrafromanultra-lowconcentrationofasam- ple, for molecules adsorbed on roughened metal surfacesof silver and gold it can be enhanced by up to 14 orders of magnitudebymeansofsurface-enhancedRamanspectrosco- py(SERS).Thisevenincludessinglemoleculedetection[3,4].Asaresult,Ramancross-sectionsofmoleculesinteracting withSERS-activesubstratescanreachvaluescomparableto those observed for the fluorescence phenomenon [3].SERS has been dynamically developing, especially in the field of bioanalysis, due to its ultrasensitive detection limits [5,6].Moreover,informative SERS signals from the intracellular microenvironmentcanbecollectedwithinsecondsincontrast tonormalRamanscattering[7].Gold-supportedinvitroSERS in living cells provides a tool for sensitive and structurally- selectivedetectionofnativechemicalssuchasDNA,proteins, lipidsetc.,andformonitoringtheirintracellulardistributions.However,the distribution of bare metal nanoparticles in the cellscannotbecontrolled[7–9].AnotherapplicationofSERS for cellular studies is based on nanoprobes conjugated toRamanreporters[5,8–11].Themostcommonlyused
ElectronicsupplementarymaterialTheonlineversionofthisarticle(doi:10.1007/s00604-014-1307-5)containssupplementarymaterial,whichisavailabletoauthorizedusers.
A.Jaworska:T.Wojcik:K.Malek(*):M.Kepczynski:
S. Chlopicki:M. Baranska
JagiellonianCentre for ExperimentalTherapeutics(JCET),JagiellonianUniversity,Bobrzynskiego14,30-348Krakow,Poland e-mail:malek@chemia.uj.edu.pl
A. Jaworska:K. Malek:U. Kwolek:M. Kepczynski:
A. A. Ansary:M. Baranska
FacultyofChemistry,JagiellonianUniversity,Ingardena3, 30-060Krakow,Poland
S. Chlopicki
DepartmentofExperimentalPharmacology,JagiellonianUniversity MedicalCollege,Grzegorzecka16,31-531Krakow,Poland
ORIGINAL PAPER

120
A. Jaworska etal.
reportersareorganicdyes,e.g.malachitegreen,rhodamineB or crystal violet[5–9].
Ontheotherhand,nowadaysconfocallaser-scanningmi- croscopy (CLSM) is a widely used technique for cellular imaging and biomedical diagnostics [12,13].Fluorescence- CLSM is the most appropriate method of imaging cells and subcellular structures, both in vitro and in vivo, once a cell showsintrinsicfluorescenceorislabelledwithafluorescent probe [14]. In comparison to the conventional fluorescencemicroscopy,CLSM reduces the effect of light scatteringen- abling the observation of thick and light-scattering objects with a good quality [13,15]. Depending on the numerical aperture of the objective, the excitation wavelength, andthe medium refraction index, the spatial resolution in thelateral andaxialdirectionscanbeasmuchas250nmand>600nm, respectively [13–15]. Furthermore, this microscopic tech-niqueallowsthereconstructionoftheoriginalthree-dimensional structure of the objects in the specimen [13,16].Asaconsequence,CLSMinfluorescencemodeprovides information on distances between specific structures in the cellsandenablesimagingofcellularcompartments[16]and monitoringphysiologicalparametersandcellularmetabolism [12]. Despite the obvious advantages, CLSM has several limitations such as photodamage and photobleaching of the sample [12,14,15].
Inthis workbothSERS andfluorescence microscopy areemployed to study intracellular environment of endothelialcells.Theendotheliumis amonolayerofcells liningofall bloodvessels(arteries,veinsandcapillaries)andthelymphatic system,and thus thisis in adirect contactwithblood/lymphandcirculatinginblood cells [17].Currently,this type ofthe cellsisrecognizedtobeapredominantplayerinthecontrolofbloodfluidity,platelet aggregation, thrombosis, vascular tone. Endothelium regulatesalso immuneresponse, inflammationandangiogenesis[18].Therefore, endothelial dysfunction,atermthatencompasses multiple potential defectsoftheendo-thelial cells, can tip the balance toward thrombosis and inconsequencethiscontributestovariouspathologicalstatessuchasatherothrombosis, arterial thrombosis (stroke, visceral and peripheral artery occlusive diseases)andthromboticmicroan-giopathies [17].Takingintoconsiderationtheimportance of endotheliumintheregulationofcardiovascular system,noveltoolsseemmandatorytofoster studiesonbiochemistry and functionofendothelialcells.
However,amajorchallengeofcellularstudiesintermsof SERS is the delivery of target nanoparticles in sufficient quantities to acquire a spectral signal allowing for simulta- neous spatial distribution of the nanoparticle (through a re- portersignal)andchemicalinformationofthecellularenvi- ronment (via the enhancement of Raman signal ofbiomole- cules on a metallic support). Therefore, the SERS- and fluorescence-based studies on the uptake of rhodamine 6G conjugated to gold nanoparticles (R6G-AuNPs) bylive
endothelial cells have been undertakeninourlaboratory.Rho- damine6Gisafluorophoreofahighcross-sectionforRaman scatteringusedbyusbeforeincellularstudiesofmacrophagesand endothelial cells [8,9]. For in vitro culture we choseEA.hy926cells, a linederivedfrom humanumbilicalveinendothelial cells.Ourpreliminary investigations haveshownvariationinSERSinformationonbiocomponentsinthiscelllinealongwithelongationofincubationtime [8].Thus,we continue our SERS studies with a support of fluorescencemicroscopy since rhodamine6Galso exhibitsahighcross- sectionfor thefluorescence phenomenon. This allowsustofollow cellular uptakeofR6G-AuNPsanddistributionofthe Raman reporter insidethecell.Finally,wedemonstrateapo-tentialapplicationofthislabelforprobingliveendothelialcells.
Materials and methods
Materials
Rhodamine6G(R6G),gold(III)chloridetrihydrate,sodium citrate tribasic dihydrate and paraformaldehyde were pur- chased from Sigma (www.sigmaaldrich.com) and were of analyticalgrade.
Anaqueousstocksolutionofrhodamine6Gattheconcen- tration of 10−3M was prepared by diluting an appropriate amount of the solid in the 4-fold distilledwater.Goldnano-
particles(AuNPs)werepreparedaccordingtotheFrenspro- cedure [19]. In this synthesis Au ions are reduced by citrate ions.R6G-AuNPssolutionwaspreparedbymixing10μLof
the1×10−3MsolutionofR6Gwith1mLofthegoldcolloid.
CellsandprotocolofSERSandfluorescenceexperiment
Experiments were conducted for EA.hy926 cells, a line de- rivedfromhumanumbilicalveinendothelialcellsfusedwith the A549 line [20]. Cells were grown in 6-well plates inDMEMsupplementedwith10%fetal bovineserum,2 mM L-glutamine, penicillin, streptomycin, and 2 %HAT.After 24 h passaging a medium was replaced by a medium containingsolutionofR6G-AuNPs.After5min,mediumwas mixedwiththeR6G-AuNPssolution(10:1v/v).Thefinal
concentrationofR6GandAuNPsinmediumwas1×10−6and 1×10−11M,respectively.Cellswereincubatedinthemedium
containingR6G-AuNPsfor0.5,1,2,4and16h.Twocontrol experimentswerecarriedouttoexcludeautofluorescenceof cellsandtoexcludethecontributionofnormalRamansignal ofthedyenon-conjugatedtoAuNPs.Cellswereincubatedin apuremediumandamediumcontainingapureR6Gsolution
(c=1×10−6M),respectively.Then, the medium was washed outthreetimeswithDPBS(Dulbeccos’sphosphate-buffered
saline)andcellswerekeptinapuremediuminanincubatoruntil SERSand2Dfluorescence measurementswere

Rhodamine6GconjugatedAunanoparticlesforSERSofcells
121
performed.For3Dfluorescencemeasurements,cellswerefixed with4%paraformaldehydefor6minandstoreinafridgeuntil measurements.For the allfluorescence measurements, nucleiwereadditionallystained with Hoechst 33342[21].
solutionin aglasscuvette.For Ramanmapping, raster scansover single living cells were carried out with a computer-controlledx,y-stage.Themappingstep was1μm.
Analysis of SERSmaps
CellmetabolicactivitybytheMTTassay
Hierarchical K-means cluster analysis of SERS images was performed by using aWITecProject 2.06 software. The spectrawereanalysedintheregionof200–1,800cm−1after a routine procedure for cosmic rays removal andsmoothing (13 points) using a Savitzky–Golayalgorithm.
CellswereexposedtoR6GandR6G-AuNPsfor0.5,1,2,4, and16h.Then,themediumwasreplacedbya2mLmedium
containing0.5mg⋅mL−1of3-(4,5-dimethyl-2-thiazolyl)-2,5-diphenyl-2H-tetrazolium bromide (MTT) followed byincu-
bation cells for 3 h at 37 °C. Afterwards, the medium was carefully removed from the wells. DMSO:ethanol (1:1)was addedtoeachwellandtheplatewasshakedonaplateshaker for 5 min to dissolve formazan crystals. Absorbance of formazan was measured at 560 nm by a BiotecSynergy™4 plate reader(www.biotek.com).
Resultsanddiscussion
SpectralcharacterisationofR6G-AuNPs
Instrumentation
AnimportantstepinthesynthesisofSERSlabelsisselection ofanappropriatemetalsurface.Themetallicsupportshould bestable,smallenoughtoeasilycrossthecellularmembrane, and cause a relatively low cytotoxicity. In our work gold nanoparticleswiththeaveragediameterof40nmwerecho- sen.TheDLS(DynamicLightScattering)methodconfirmed
Theelectronicabsorptionspectraofthegoldcolloid,theR6G solutionandthegoldcolloidmixedwithR6Gwererecorded withaUV–vis-NIRPerkinElmerspectrophotometer(model Lambda 35)(www.perkinelmer.com)in the range of 190–1,100 nm with a resolution of 2 nm. Quartz cells of 1 cm wereused.
Fluorescenceimagesofcellsforthequantitativeanalysisof fluorescence were collected using Olympus Scan^R system(www.olympus-europa.com)in DAPI and Cy3 channels for Hoechst33342andrhodamine6G,respectively.Imageswere constructed by using Columbus data storage and analysis system (Perkin Elmer). 3D fluorescence images of R6G- AuNPs-incubated cells were acquired with a A1-Si Nikon (Japan) confocal laser scanning system built onto a Nikon inverted microscope Ti-E using a Plan Apo 100×/1.4 Oil DICobjective(www.nikon.com).Imageswererecordedata resolution of 1,024×1,024 while Hoechst 33342 and R6G wereexcitedwith405and561nmdiodelasers,respectively.3D fluorescence images were constructed by using a NIS- Elements AR 3.2software.
SERSmappingofcells and SERSspectraofR6G-conjugated AuNPswerecarriedoutbyusingaWITecsystem(www.witec.de),equippedwithanimmersive objective withmagnification of 60× and a He-Ne laser (632.8 nm). Thisoptical setting providesmax.spatial resolutionof0.4μm. For allmeasurements, integrationtime was 0.05swithasingle
accumulation,laserpowerof10mWandgrating600g⋅mm−1.Therecorded spectral rangefor thisgratingis0–2,400cm−1. SERSspectraofR6G-AuNPsasareferenceforcellsmapping
wererecordedbyplacingasampleinaglasscuvetteandusinganairobjective(20×).ThreeSERSspectrawereacquired,eachforfreshlypreparedsample.Thelatterwaspreparedbymixing
500μL of the Au colloid with 5μL of a 1×10−3M R6G
the
size
of
AuNPs (approx.
45
nm) while
AFM images
showedclearlythesphericalshapeofnon-aggregatednano- particles (Fig. S1in Electronic Supporting Material, ESM). AccordingtoDLS,goldnanoparticlesexhibitedrelativelylow polydispersityindexof0.38.TheUV–visspectradisplaythe presenceofaLSPRbandofthecolloidat527nm,typicalfor thisdiameteroftheAusol(Fig.S2,ESM).Thenaspectrumof thedyemixedwiththegoldcolloidshowsthecharacteristics ofaggregateformationbythepresenceofextendedplasmon bandwithasecondmaximumat641nm,c.f.FigS2.Forma- tion of small aggregates results in an increase of SERS en- hancementfactors[22].Here,thechosensizeofAuNPsand concentrationofR6GprovideastableSERSsignalofthedye. Figure S3(ESM) shows the comparison of the exemplary threerawSERSspectraofR6Gadsorbedonthegoldcolloid usedfurtherinSERSmappingofcells.Positions,fullwidthat half maximum and relative intensities of SERS bands are identicalineachspectrumwhilethetotalintensityofthe
spectra in the recorded region varies withinca.7
%. This
confirms the stability of the SERS signal of the Raman re- porter resulting from a relatively similar aggregation of the gold nanoparticles.
CytotoxicityofR6GandR6G-AuNPs
A cytotoxic effect of the gold and silver nanoparticles has been previously reported [23,24]. The exposition of C17.2 neural progenitor, human umbilical vein endothelial, and PC12 rat pheochromocytoma cells to AuNPs at the

122
A. Jaworska etal.
concentrationof100nMfor24hdidnotinduceacutecyto- toxicityasactivityoflactatedehydrogenase(LDH)revealed whiledeformationofactinandtubulincytoskeletonwasob- servedfor50nMconcentrationofAuNPs[24].However,this effectistime-andconcentration-dependentaswellasitcanbe specific for a type of cells. In our work, we used a lower concentration of AuNPs (10 pM in medium) than in the literature[24],thereforeweexcludedatoxicinfluenceofthe goldnanoparticlesontheEA.hy926cells.Next,weevaluated toxicity of R6G and R6G-AuNPs by performing the MTT assay(Table1). The MTTassay,which is sensitive to mito- chondrialactivity,exhibitsnotonlycellapoptosisbutalsothe inhibitionofcelldivision.TheEA.hy926cellsaresensitiveto rhodamine 6G after long incubation time whereas the pres- ence of both the dye and the gold nanoparticles affects the cellsevenafter1-hcontact.Non-toxiceffectoftheSERSlabel isobservedupto4handthenmassiveapoptosis/necrosisof theendothelialcellstakesplaceafter16hofincubation.This indicatesthatEA.hy926cellscanbeexposedtonanocarriesin a relatively short time of a fewhours.
required to saturate the endothelial cells by the dye, 2/ differences in kinetics of the uptake, consequently in themembranetransport,betweenconjugatedandnon-conjugated molecules of the dye, and finally 3/ the con-tributionof theactive (involving cellularenergy)andpassive (a diffusive process) mechanism into the mem- brane transport of the endothelium. An overall summary of the kinetics of the uptake of non-conjugated and con- jugated R6G molecules for the EA.hy926 cells is given in Fig.1. During uptake of the dye, the fluorescence rises quite quickly on the timescale of 30 min in comparison to the control group indicating the presence of rhodamine 6G in the intracellular compartments of endothelial cells, and then the intensity of fluorescence emission for R6G continues to grow up to 2 h. With a longer than 2 h incubation time, it is maintained at a relatively similar level indicating that saturation of the cells by the dye takes place within 2 h. In terms of the export oftheRaman reporter from the endothelial cells, a very slow decay process can occur after 16 h as an insignificant fluorescence decrease is found for this incubation time.Moreover, the fluorescence emission is very similar for both R6G and R6G-AuNPs on the whole timescale used in our protocol. This undoubtedly confirms the intracellu- lar transport of a similar amount of the dye regardless of its binding to the gold nanoparticles in the medium. How- ever, these data do not indicate whether the R6G-AuNPs or the bare R6G molecules are transported through the cellular membrane since the technique is not sensitive to the metallic SERS support. This will be confirmed by SERSmappinginthesectionbelow.
Toassesswhatmechanism,i.e.cellularchemical–mechan- ical energy or a simple diffusion process, plays a dominant role in the uptake of the dye/nanoparticles, thefluorescence wasmeasuredforcellculturesat25and4°C(Fig.S4,ESM).Unfortunately,endothelialcellsareverysensitivetothetem- peraturestressandafter1hthecellularnecrosisoccurredat roomtemperature.Forcellsincubatedat4°Cwewereableto carryoutfurthermeasurementsevenafter4h.At4°Callthe cellularprocessesareslower,sothenecrosisprocessappears later comparing to 25°C.
The average intensity of fluorescence emission for cellsincubatedwithR6G-AuNPsaswellaswith R6Gfor30 min at 37, 25 and 4 °C is 265/283, 217/203 and 221/ 221 [in relative fluorescence intensity], respectively for R6G-AuNPs/R6G, while the control group exhibits auto- fluorescence with the intensity of 193 regardless of tem- perature (Fig.1and Fig. S4, ESM). These results indicate that no clear trend can be found between the uptake of R6G and R6G-AuNPs at a given temperature in short timeoftheincubation.Thefluorescenceonlyslightlyde-creases along with inducing energy depletion. After the 1 h incubation, a higher concentration of R6Gconjugated
TheuptakeofR6GandR6G-AuNPsbyendothelialcells:2D quantitative intracellularfluorescence
A crucial step in the application of the dyes and nanopar- ticles in detection of intracellular chemical environment is determination of the uptake mechanism of non-conjugated and conjugated dye molecules to Au nanoparticles. For this purpose 2D quantitative fluorescence spectroscopy can be used to determine an amount of a labile fluorescent reporter inside cells. However, such information cannot be achieved for the bare metal nanoparticles as they do notpossessthefluorescent features.In ourapproach,weemployed incubation time from 0.5 till 16 h (0.5, 1, 2, 4 and 16 h)keeping cellsin anoptimal temperatureof 37 °C as well as under energy depletion conditions at 25 and4°C.Thisexperimentshouldshow:1/whattimeis
Table1Cell viability determined by a MTT assay for cells incubated withR6G-AuNPsandR6Gintimeintervals.Controlcellswereincubat- ed with a puremedium
Incubationtime[h]
Concentrationofformazan[%ofcontrol]
R6G-AuNPs
R6G
0.5
1
2
4
16
Control
97
79
73
77
37
100
100
100
90
90
83
100

Rhodamine6GconjugatedAunanoparticlesforSERSofcells
123
Fig.1ThecomparisonofR6G-AuNPs(green)andR6G(yellow)uptakebyEA.hy926endothelialcellsfor0.5–16hin37°C.Controlcells(blue)were incubatedinalabel-freemedium.Therelativefluorescenceintensitiesareprovidedalongwithstandarddeviationbars
to the gold nanoparticles than the bare R6G is found in the endothelial cells incubated at 37 and 25 °C sincerelativefluorescence intensitiesare338/290and260/238, respectively. The results also suggest that a principal mechanism of cellular uptake of R6G-AuNPs but not of R6G is an energy-dependent process of endocytosis. It is well known that the mechanism of endocytosis dependsonthesizeofmaterialand for NPs withadiametersmaller than 40 nm, the docking of the NPs does not produce enough energy to completely wrap the NPs by the cell membrane [26,27]. In our work, the gold nano- particles are of aca. 40 nm diameter and they aggregate after mixing with the Raman reporter. Moreover, a very slight increase in fluorescence in comparison to the con- trolgroupisobservedforthecellsincubatedat4°C(212/
226 forR6G-AuNPs/R6G).Inthis case, however,thefluorescence intensity has no obvious change compared to that observed for the 0.5-h incubation but it increases after 2 h,c.f.Fig. S4B(ESM), indicating a slow diffusion process. At the present stage, it is very hard to clarify whether the difference in the fluorescence results between the cells with R6G-AuNPs and R6G is statistically signif- icant(approx. 250–300 cells measuredperwell).Thecellular delivery of R6G-AuNPs to the endothelium via active and passive mechanisms may occur simultaneously in our experiment leading to the saturation of the cells after 2–4h.
The 2D intracellular fluorescence measurements of cells with the use of a high-content screening automated
microscope enable the quantitative analysis of a dye for a large cell population [28,29], however, this technique does not determine an exact location of the dye molecules in the intracellular compartment. Figure2illustrates fluo- rescence image of the EA.hy 926 cells with the Hoechst-stained nucleiandyellow stainingof R6Gdistributedwithin cytoplasm. It is rather impossible to asses from this image whether the R6G molecules are present inside thecells,orpossibly theyaresimply attachedtothemembrane surface of theendothelial cells.
Fig.2Therhodamine6GmoleculesdetectedincytoplasmofEA.hy926 endothelial cells by 2Dfluorescence microscopy.Nuclei stained with Hoechst 33342 are blue, R6G isyellow

124
A. Jaworska etal.
Fig.33Dconfocalfluorescenceimagesofendothelialcellsincubatedfor2hwithR6G-AuNPs.Blue:nucleistainedwithHoechst,red:rhodamine6G. The right bottom image shows the distribution of R6Gonly
ThelocationofR6Gintheendothelialcells:3Dconfocal fluorescence
from the corresponding classes. The SERS bands of rho- damine 6G are observed in the spectra recorded for the incubation time up to 2 h. Their distributions inside the cells shown in the cluster maps implicates a decrease in the concentration of the R6G-AuNPs particles upon long incubation time and moving them towards the cell mem- brane,cf.pink traces in Fig.4a–c. On the other hand, since the SERS spectra for each incubation time exhibit the presence of bands attributed to various biomolecules(discussedbelow),the R6Gmoleculesmustbede-attached from the surface of the gold and then biomole- cules present in the close vicinity of hot spots exhibitSERS signal. In our preliminary studies on probing cellu- lar environment of the endothelium by the R6G-AuNPs label, we observed the SERS signal of the dye for the 2- and 6-h incubation time while SERS bands originating from various biomolecules were observed up to 16 h [8]. This indicates that the conjugation of rhodamine 6G to nanoparticles can be stable up to a few hours. Salvati et al. have shown that after the uptake of nanoparticles containing a high concentration of a labile dye, the dye molecules are randomly spread across the intracellularspace whereasthe dyeconjugatedtonanoparticlesisspatially localised [25]. A similar effect is observed in our experiment. As the 3D fluorescence image showed above, the labile R6G molecules fill up the cytoplasm, probably reaching the endosomes of the cell whereas the distributionofR6G-AuNPsinSERSmapsislocalised.
ApartfromSERSbandsofR6G,meanSERSspectrashow the presence of marker bands of cell biomolecules assigned according to the literature,seeFig.4[8,9,29,30]. In the spectraofthecellsincubatedfor30min.,bandsattributedto
proteinsandlipids(1,268,1,278,1,464,1,545cm−1)andthe
3Dconfocalmicroscopywasemployedtoconfirmtheintra- cellular uptake of R6G-AuNPs by the endothelial cells. Figure3illustrateslocationofthenucleussurroundedbythe dye spread throughout the cell without entering to the nucleus. The changes in the fluorescence intensity show that small aggregates of the Raman reporter dye are dis- tributed unevenly in the cytoplasm but it is rather impos- sible to determine if they are localised in specific cell compartments.
Chemicalinformation:SERSmappingoftheendothelialcells
As shown above, the fluorescence provides information on thecellular distributionofrhodamine6G butthistechnique does not differentiate the bare and conjugated dye so it is difficult to follow the presence/absence of R6G conjugated to AuNPs.Toinvestigate this as well as to analyse potential chemical information gathered from molecular vibrations of biomolecules, surface-enhanced Raman mapping was performed for the endothelial cells incubated with R6G-AuNPs. The control groups were the cell cultures incubated in the label-free medium as well asinthemedium containingR6G. For bothgroups,noRaman signal was recorded indicating that the use of the 633 nm laser excitation and short integration time (0.05 s) do not provide intracellular chemical information without a SERS support (data not shown). This has been also reported by Sathuluri et al. [30]. Figure4illustrates mi- croscopic images of representative cells along with K- meansclustermapsandmeanSERSspectraextracted

Rhodamine6GconjugatedAunanoparticlesforSERSofcells
125
Fig. 4SERS mean spectra extracted from cluster maps of endothelial cells incubated with R6G-AuNPsfor0.5h(a),1h(b),
2h(c),4h(d),and16h(e)along withamicrophotographyofacell andaclustermap.Blacktracein
(c) represents a reference SERS spectrum of rhodamine 6G. The colours of spectra correspond to the colours of classes in the cluster map
phosphategroups(419,814cm−1)arefound(Fig.4a).After the1-hincubation,proteinandlipidbandsarestillobserved (at 1,271, 1,442, 1,461, 1,657 cm−1) along with Raman markers for tyrosine (631, 823 cm−1) and the C-C and C-N stretchingvibrations(1,156cm−1),c.f.Fig.4b.Inturn,afew bandsoriginatingfromCys(664cm−1),Trp(760cm−1)and
Phe(1,001and1,021cm−1)appearinSERSspectrumofthe cellsuponthe2-hincubationwithR6G-AuNPsbutthisspec- trumismainlydominatedbytheR6Gsignal(Fig.4c).Forthe
4 and 16-h incubation (Fig.4d, e), we identified bands of amino acid residues such as cysteine (502 cm−1), tyrosine
(658, 838 cm−1), proline (931 and ca. 1,130 cm−1)
and

126
A. Jaworska etal.
purines/pyridines (1,228, 1,268, 1,314, 1,516 cm−1). Summarizing, the SERS label containing R6G as a Raman reporter enables sensitive and locally confined
chemical probing of intracellular environment indicating mainly the presence of amino acid residues and moieties of nucleicacids.
Development Fund under the Innovative Economy Programme (grantcoordinatedbyJCET-UJ,NoPOIG.01.01.02-00-069/09).Wealso thank DrM.OcwiejafromtheJerzyHaberInstituteofCatalysisandSurface Chemistry(PolishAcademyofScienceinKrakow)forAFMmeasure- ments and Msc. Eng. A. Szpak (Faculty of Chemistry, Jagiellonian University in Krakow) for DLSmeasurements.A.J. thanks Prof. H.J. Byrne from the Focas Research Institute in Dublin for the creative discussion.Theresearchwascarriedoutwiththeequipmentpurchased thankstothefinancialsupportoftheEuropeanRegionalDevelopment Fund in the framework of the Polish Innovation EconomyOperationalProgram (ContractPOIG.02.01.00-12-023/08).
Conclusion
OpenAccessThisarticleisdistributedunderthetermsoftheCreativeCommonsAttributionLicensewhichpermitsanyuse,distribution,and reproduction in any medium, provided the original author(s) and the source arecredited.
The work demonstrates a detailed and multiparametric ap- proachtoassesstheinteractionsoftheendothelialcellswith the gold nanoparticles immobilized with the Raman report- er—rhodamine 6G.Firstly,we show that the designedparti- clescaninterferewithnormalcellularhomeostasiswithin4h, leadingtosubstantialtoxiceffectafter16h.Thissuggeststhat although a non-toxic concentration of AuNPs is used in the experiment, their conjugation with a Raman reporter can induce cytotoxic mechanism in the endothelium especially duringthelong-timeincubation,furtheremphasizingtheim- portance of evaluating the toxic effects of nanomaterials on cultured cells. Then, we employ the chosen nanoparticlesto studythecellularuptakebehaviourofR6G-AuNPsbymeans of2Dand3DfluorescenceandSERSspectroscopy.Wereveal thattheuptakeofthedyeaswellasthedye—Ausupportisa relatively fast process in that the cell is saturated by both specieswithin2handtheyareaccumulatedinthecytoplasm withoutanindicationofaspecificcellularcompartment.The current work suggests that the mechanism of the cellular uptake is energy-dependent endocytosis.However,specific pathways of such a mechanism must be studiedseparately.In turn, intracellular SERS imaging provides the strong and stable signal of cellular components of the endothelium exhibiting the presence of amino acid residues and bases of nucleicacids.ThecomparisonofbothSERSandfluorescence imagingclearlyshowsthattheRamanreporterisde-attached from the surface of SERS substrate in the intracellularenvi- ronment already after 0.5 h of the incubation since SERS signal of biomolecules is observed. This may implicate a real-timeprocessofexchangingadsorbatesinthelocaloptical field of the metal nanoaggregates and/or rearrangement of gold nanoaggregates in a way in which SERS hot spots are formedaroundothermoleculesthanthedye.Insummary,ourstudiesalsodemonstratethestrengthofamulti-methodological approach for in vivo cell labelling applica- tionsandmayprovidehintstoestablishareferenceprotocol forfurtherstudiesinvestigatinginteractionsbetweencellsand nanocarries.
References
1. Auchinvole CAR, RichardsonP,McGuinnes C, MallikarjunV,DonaldsonK,McNabH,CampbellCJ(2012)Monitoringintracel-lularredoxpotentialchangesusingSERSnanosensors.ACSNano6: 888
2. Leopold N, Baena JR, Bolboaca M, Cozar O, KieferW,Lendl B (2004) Raman, IR, and surface-enhanced Raman spectroscopy ofpapaverine.An automated setup for in situ synthesis of the silver substrateandrecordingoftheSERspectra.VibSpectrosc36:47
3. CulhaM,CullumB,LavrikN,KlutseCK(2012)Surface-enhancedRaman scattering as an emerging characterization and detection technique. J Nanotechnol12:1
4. JaworskaA,MalekK,MarzecKM,BaranskaM(2012)Nicotinamide and trigonelline studied with surface-enhancedFT-Ramanspectroscopy.VibSpectrosc63:469
5. KneippJ,KneippH,KneippK(2008)SERS—asingle-moleculeand nanoscaletoolforbioanalytics.ChemSocRev37:1052
6. GuoX,GuoZ,JinY,LiuZ,ZhangW,HuangD(2012)Silver–goldcore-shellnanoparticlescontainingmethyleneblueasSERSlabels forprobingandimagingoflivecells.MicrochimActa178:229
7. Kneipp K, Haka AS, Kneipp H, Badizadegan K,YoshizawaN, Boone C,Shafer-PeltierKE, MotzJT,Dasari RR, Feld MS (2002)Surface-enhanced Ramanspectroscopyin single living cells using gold nanoparticles. Appl Spectrosc56(2):150
8. JaworskaA,MalekK,Kachamakova-TrojanowskaN,ChlopickiS, BaranskaM(2013)Theuptakeofgoldnanoparticlesbyendothelialcells studied by surface-enhanced Raman spectroscopy. Biomed Spectrosc Imaging2:183
9. Malek K, Jaworska A, KralaP,Kachamakova-Trojanowska N, BaranskaM(2013)ImagingofmacrophagesbySurfaceEnhanced RamanSpectroscopy(SERS).BiomedSpectroscImaging2:349
10. SchluckerS(2011)SurfaceenhancedRamanspectroscopy.WILEY-VCHVerlagGmbH & Co. KgaA, Germany
11. KneippJ,KneippH,RajaduraiA,RedmondRW,KneippK(2009)OpticalprobingandimagingoflivecellsusingSERSlabels.JRaman Spectrosc40:1
12. HalbhuberKJ,KonigK(2003)Modernlaserscanningmicroscopyinbiology,biotechnology and medicine. Ann Anat185:1
13. PygallSR,WhetstoneJ,TimminsP,MeliaCD(2007)Pharmaceuticalapplicationsofconfocallaserscanningmicroscopy:thephysicalcharacterisationofpharmaceuticalsystems.AdvDrug Deliv Rev59(14):1434
14. FischerRS,WuY,KanchanawongP,ShroffH,WatermanCM(2011)Microscopyin3D:abiologist’stoolbox.TrendsCellBiol21(12):682
AcknowledgmentsThis work was supported by National Center of Science(DEC-2013/08/A/ST4/00308andDEC-2012/05/N/ST4/00218)
andbytheEuropeanUnionfromtheresourcesoftheEuropeanRegional

Rhodamine6GconjugatedAunanoparticlesforSERSofcells
127
1. ConchelloJA,LichtmanJW(2005)Opticalsectioningmicroscopy.Nat Methods2(12):920
2. Foldes-PappZ,DemelU,TilzGP(2003)Laserscanning confocalfluorescence microscopy:anoverview.IntImmunopharmacol3:1715
3. FélétouM(2011)Multiplefunctionsoftheendothelialcells.In:The endotheliumpart1:multiplefunctionsoftheendothelialcells—focus onendothelium-derivedvasoactive mediators.Morgan& ClaypoolLife Sciences, SanRafael
4. Wnuczko K, Szczepanski M (2007)Endothelium—characteristicsand functions. Pol Merk LekXXIII(133):60
5. Frens G (1973) Controlled nucleation for the regulation of the particle size in monodisperse gold suspensions. Nat Phys Sci241:20
6. Edgell C, McDonald C, Graham J (1983) Permanent cell line ex- pressinghumanfactorVIII-relatedantigenestablishedbyhybridiza-tion. Proc Natl Acad Sci80:3734
7. OttoF,TsouKC(1985)Acomparative studyofDAPI, DIPI,andHoechst22358and33342aschromosomalDNAstains.StainTechnol60(1):7
8. JosephV,Matschulat A, Polte J, Rolf S, EmmenrlingF,Kneipp J(2011)SERS enhancement of gold nanospheres of defined size. JRaman Spectrosc42:1736
9. Asare N, Instanes C, Sandberg WJ, Refsnes M, SchwarzeP,KruszewskiM,BrunborgG(2012)Cytotoxicandgenotoxiceffects ofsilvernanoparticlesintesticularcells.Toxicology291(1–3):65
1. Soenen SJ, Manshian B,MontenegroJM, AminF,Meermann B, ThironT,CornelissenM,VanhaeckeF,DoakS,ParakWJ,DeSmedt S,BraeckmansK(2012)Cytotoxiceffectsofgoldnanoparticles:amultiparametricstudy.ACS Nano6(7):5767
2. SalvatiA,AbergC,dosSantosT,VarelaJ,PintoP,LynchI,Dawson KA(2011)Experimentalandtheoreticalcomparisonofintracellular import of polymeric nanoparticles and small molecules: towardmodels of uptake kinetics. Nanomedicine7(6):818
3. WangSH, Lee ChW,Chiou A,WeiPK (2010) Size-dependent endocytosisofgoldnanoparticlesstudiedbythree-dimentionalmap-pingofplasmonicscatteringimages.JNanobiotechnol8:33
4. HuangJ,ZongC,ShenH,LiuM,ChenB,RenB,ZhangZ(2012) Mechanismofcellularuptakeofgraphemeoxidestudiedbysurface-enhanced Ramanspectroscopy.Small8:2577
5. Xu Z, Huang X, Dong C, Ren J (2014) Fluorescence correlation spectroscopy of gold nanoparticles, and itsapplicationto an aptamer-based homogeneous thrombin assay. Microchim Acta181:723
6. KneippJ,KneippH,McLaughlinM,BrownD,KneippK(2006)In vivomolecularprobingofcellularcompartmentswithgoldnanopar-ticles andnanoaggregates.Nano Lett6(10):2225
7. Sathuluri RR,YoshikawaH, Shimizu E, Saito M,TamiyaE(2011)Goldnanoparticle-basedsurface-enhancedRamanscatteringfornon- invasivemolecularprobing of embryonic stem celldifferentiation.PLoS One6(8):e22802