ColloidsandInterfaceScienceCommunications2(2014)11–14
Rapid Communication
Effect of Zn2+Concentration on the Adsorption of Organophosphonic Acids on Nanocrystalline ZnO Surfaces
A. Pomorska1, G. Grundmeier, O. Ozcan⁎
Technical, Macromolecular Chemistry, University of Paderborn, Warburgerstr., 100 D-33098 Paderborn, Germany
article	i n fo
a b s t r a c t
TheeffectofthepresenceofZn2+ionsontheadsorptionofoctadecylphosphonicacid(ODPA)onnanocrystallineZnOﬁlmshasbeenstudiedbymeansofQuartzCrystalMicrobalance(QCM)techniqueandcomplementaryex- situanalysisofﬁlmproperties.Phosphonicacidmoietyhassufﬁcientacidity,eveninorganicsolvents,tocause dissolution of ZnO. Dissolved Zn2+ions form complexes with the ODPA molecules in the solution, leading to thedepositionofthickandundeﬁnedprecipitationlayers.Ourresultsindicatethattheformationofsuchprecip- itationlayerscouldbepreventedbytheadditionofappropriateamountsofZn2+ionsintothedepositionsolu- tion. Bi-functional monomolecular linkers with phosphonic acid head-groups are excellent candidates forapplication-speciﬁcfunctionalizationofnanostructuredZnOﬁlmsaswellasZnOnanoparticles.Theresultspre- sented here demonstrate a straight forward method to increase theﬁlmquality.
© 2014 Published by Elsevier B.V. This is an open access article under the CC BY-NC-ND license
(http://creativecommons.org/licenses/by-nc-nd/3.0/).
Article history:
Received 21 April 2014
Accepted 25 August 2014
Available online 23 October 2014
Keywords:Nanocrystalline ZnOﬁlmsOrganophosphonicacids ZnOdissolutionZincoxide
self assemblySAMs
AdsorptionHydrophobicityQCM
FT-IRRAS
Synthesisandfunctionalizationof ZnOnanocrystallineﬁlms have in-vokedgreatattentiondue to their high potential asfunctional materialsinoptics, catalysisor aselectrode materialin solar cells[1–4].Recently,thepositiveeffect of suchﬁlmsoncorrosionandadhesion propertiesof zinc surfaces and the fabrication of nanocrystalline ZnO based high- sensitivity sensors has been reported[5–11]. With their single crystal- line nature and controllable morphology, nanocrystalline ZnOﬁlms can also provide a well-deﬁned model system for the fundamental in-vestigationofcorrosionandadhesionprocesses.
Functionalizationof zinc oxidenanocrystallineﬁlmswith ultra-thin organicﬁlmsis a promisingmethodfor theapplication-speciﬁc adjust-ment of the surface chemistry[12–14]. Application of alkanethiolate SAMs on metal surfaces,especiallyAu and Cusurfaces,has been exten- sively studied[15–17]. The adsorption of organosilanes and organic acidssuchascarboxylicandphosphonicacidsiswellestablishedonvar- ious metal oxides, such as Al2O3, TiO2and ZnO[18–20].
It is known from the literature that Zn2+ions can form complexes withphosphonicacidfunctionalmolecules. This effect was used inliq-uid–liquid Zn2+extraction technology by employing bi-functional or- ganophosphorus species[21]. Moreover, Wong et al. have shown that phosphonic acids slow down the growth rate of ZnO nanoparticles, by
adsorbingontheirsurfaceandprovidingabarrierforfurtherdissolution[22]. In a recent publication, Zhang and co-workers have studied the surface functionalization of ZnO nanowires and ZnO (0001) single crystalline wafers with 3-Phosphonopropionic acid (3-PPA) and 10-Phosphonodecanoic acid (10-PDA) and have reported an increase of surface roughness as well as inhomogeneousﬁlm formation in case of 3-PPA, which they have attributed to the acidic etching of the ZnOwafersurfaceduringtheadsorptionprocess[12].
This paper aims at the clariﬁcation of the adsorption process of alkylphosphonic acids on ZnO nanocrystallineﬁlms by means ofQuartzCrystalMicrobalance(QCM) andex-situ analysisofﬁlm chemis- try andmorphology.ZnOnanorodﬁlms were deposited on gold coated quartzcrystalelectrodes.Toensureahomogeneousanddensenanorodﬁlm growth, the QCM crystals have been covered with a zinc oxide seed layer. Freshly cleaned QCM crystals (H2O:H2O2:NH3, 1:1:1 at 75 °C for 1 h) were wet with a 5 mM ethanolic (N99.9%, Berkel AHK Alkoholhandel, Germany) solution of zinc acetate dihydrate (Zn(O2CCH3)2(H2O)2, 98% ACS, Alfa Aesar, Germany) for 10 s, rinsedwithethanolanddriedwithastreamofnitrogen.Thisstepwasrepeat-edﬁvetimesfollowedbyanannealingstepat350°Cfor8hforthether- maldecompositionofzincacetatetozincoxide[23].Inordertoensurea homogeneous seed layer coverage, this procedure was repeated twotimes.ZnOnanocrystallineﬁlmgrowthhas beenperformedin a0.05M aqueous solution of zinc nitrate, Zn(NO3)2·6H2O (99+%Puratonic, Alfa Aesar, Germany) and hexamethylenetetramine (HTMA) C6H12N4(99+%,AlfaAesar,Germany).Thecontinuousnanocrystalline
Corresponding author. Tel.:+495251605725.
E-mail address:Ozcan@tc.uni-paderborn.de(O. Ozcan).
1Presentaddress:FacultyofChemistry,JagiellonianUniversity,Ingardena3,30-060, Krakow, Poland.
http://dx.doi.org/10.1016/j.colcom.2014.08.004
2215-0382/©2014 Published by Elsevier B.V. This is an open access article under the CC BY-NC-ND license(http://creativecommons.org/licenses/by-nc-nd/3.0/).
Contents lists available atScienceDirect

Colloids and Interface Science Communications

journal homepage:www.elsevier.com/locate/colcom

12
A.Pomorskaetal./ColloidsandInterfaceScienceCommunications2(2014)11–14
morphologywasachievedbyadditionof5mMsodiumcitrate(sodium citrate dihydrate; ACS, 99.0%, ABCR Inc., Germany) to the deposition bath[24]. The growth temperature and duration were selected as 90±2 °C and 30 min,respectively.The water used for allexperimentsin this paper was de-ionized (18.2 MΩcm resistivity) with a Purelab Plus UV (USF)ﬁltrationsystem.
QCM frequency and energy dissipation shifts were evaluated with the normalized 5th overtone (Δf25MHz/ 5,ΔΓ25MHz/ 5) to obtain moresensitiveresponsefromNR/liquidinterface.Referenceharmonics have been determined in the conductance spectra by means of QTZ software prior each experiment. Pure solvent was pumped through the cell over a ZnO coated quartz crystal sensor at a rate of 50 mL/h. After reaching a baseline, ethanolic octadecylphosphonic acid solution (1 mM)waspumpedinto the QCM cellwiththe sameﬂowrate.The ad- sorption experiment was stopped after attaining a stationary state for bothfrequencyanddissipationshifts.Subsequentlythe cell waspurgedwithpuresolventtoremoveanyunboundspecies.Fortheinvestigationof the effect of thepresenceof Zn2+ions on theadsorptionprocess 1.0 and 0.1 mM zinc nitrate salt was added into the 1 mM ODPAethanolicsolutions. For all of the studied systems the frequency and dissipation shiftsstayedconstant during the rinsingstep.
The morphology of the substrates before and after the adsorption experiments have been analysed by means of FE-SEM (NEON 40 FE-SEM, Carl Zeiss SMT AG, Oberkochen, Germany) at an accelerating voltage of 1.0 kV. Film quality and surface hydrophobicity has beenstudiedby means ofwatercontact anglemeasurements(WCA, appara- tusOCA15Plus,Dataphysics,Germany).Thereportedwatercontactan- glesaretheaveragevaluesofthreemeasurementpoints.ThechemistryoftheadsorbedﬁlmswasanalysedbymeansofFourierTransform–InfraRedReﬂectionAbsorptionSpectroscopy(FT–IRRAS)(Nicolet5700,Thermo Fisher Scientiﬁc GmbH, Germany) at 78° reﬂection angle (VeeMAX II reﬂection cell, Pike Technologies, USA) after each experi- ment and absorbance values were evaluated by taking the as- prepared ZnO samples asreference.
The frequency and energy dissipation shifts for the adsorption of
ODPAwithandwithouttheadditionofZn2+ionsarepresentedinFig.1.Highnegativefrequencyshift(Δf=−210Hz,ΔΓ=130Hz)ob-servedwiththeODPAadsorptionwithoutadditionofZn2+indicatesa complexﬁlmformationmechanisminsteadofaself-assemblyprocess. WhenZn2+ionsareaddedtotheadsorptionsolution,frequencyshifts
ofΔf=−115HzandΔf=−6HzhavebeenobservedwithZn2+con-centrationsof0.1mMand1.0mM,respectively.Thefrequencyshiftob-
served with the addition of 1 mM Zn2+is in the order of ODPA SAM formation on PVD-deposited aluminium surfaces, previously reported byGizaetal.[25].Theenergydissipationshifts,whichprobethechang-esintheviscoelasticresponseofthesolid–liquidinterface,decreased
Fig.2.FTIRspectraoftheﬁlmsformedfrom1mMethanolicsolutionofODPAonZnOﬁlm withandwithoutadditionofZn2+ions.(Thespectrawereshiftedandscaledasindicated in the graph forclarity).
fromΔΓ=130HztoΔΓ=44HzandΔΓ=5Hzwiththeadditionof 0.1 mM and 1.0 mMZn2+,respectively.
TheFTIRspectraoftheﬁlmsintheregion3000cm−1–2750cm−1are presented inFig. 2. The peaks observed at 2918 and 2848cm−1wereassignedtoasymmetricandsymmetric–CH2vibrations,respec- tively.Thepeakat2956cm−1,withaconsiderablylowintensitywas
assignedtotheasymmetric–CH3vibrationpeak.Ananalysisofpeak ratioconcerningaself-assemblyprocesswasnotpossibleduetothe morphologyoftheZnOsubstratesandcomplexityofﬁlmstructure;howeverthedecreaseinthesignalintensityof–CH2/–CH3vibrationswiththeincreaseofZn2+concentrationintheODPAsolutioncorrelates wellwith the QCMresults.
FE-SEM micrographs of the nanocrystalline ZnO substrate before and after the adsorption of ODPA with and without the addition of Zn2+are presented inFig. 3. As it can be clearly seen inFig. 3b and c, the adsorption of ODPA without addition of Zn2+ions and with the ad- dition of 0.1 mM Zn2+resulted in the deposition of the precipitationﬁlms, which would explain the high QCM frequency shifts observed in the experiments. With the addition of 1 mM Zn2+the formation of pre- cipitation layers could be prevented.
Asdescribedby Zhang andco-workers,thephosphonicacidmoiety,due to its high acidity, can cause dissolution of ZnO, even in non- aqueous solvents[12]. Thus, the formation of the web-like structures can be explained by a complex formation of the organophosphonic acidmoleculesanddissolved Zn2+ions.Bothdissolutionand complex- ation reactions should have proceeded simultaneously leading to the
Fig.1.a)Frequencyandb)energydissipationshiftsfortheadsorptionofODPAfrom1mMethanolicsolutiononZnOﬁlmandadsorptionfromsolutionscontainingadditionally0.1and
1.0 mM Zn2+ions. (The frequency and dissipation shifts obtained with the addition of 1.0 mM Zn2+ions are multiplied with 3 for clarity).

A.Pomorskaetal./ColloidsandInterfaceScienceCommunications2(2014)11–14
13
Fig.3.FE-SEMimagesofa)ZnOnanocrystallineﬁlmsubstrateb)afteradsorptionfrom1mMODPAsolutionwithadditionofc)0.1mMZn2+andd)1.0mMZn2+.
deposition of thick adsorbate layers. This would cause the kinetic data obtained by means of QCM to be the sum of a positive shift due to the ZnOdissolutionandanegativeshiftcausedbythedepositionofthepre- cipitationﬁlm. As a result the completion time ofﬁlm formation was prolonged. Observed aggregate formation of molecules carrying apolar functionalgroup and long non-polar chainwithtypicalsurfactantstructure on polar surfaces could be explained by the reduction of the contact area of non-polar hydrophobic alkyl chains in a slightly polar solvent such as ethanol[13]. Additional experiments have been per- formed to assure that the formation of the precipitationﬁlms was caused by the dissolution of ZnO at the interface. Small volumes (~ 25μl) of the deposition solution after various reaction times have been drop-casted on Si wafers by evaporating the solvent under vacu- um. The FE-SEM images of drop-casted deposition solutions are pre- sented in the supplementary material (Figure S1). As seen in Figure S1, in the presence of organophosphonic acids, Zn2+is alreadyforming similar aggregate structures in the solution phase without af- fecting the colloidal stability of the solution or causing any observable precipitation during the experiments. The drop-castedﬁlms formed with the addition of 0.1 mM Zn2+were similar to the structures ob- served on the ZnO nanocrystals after ODPA adsorption in the QCM ex-periments without the addition of Zn2+ions. However, the formation of the dense aggregates with the drop-casted 1 mM Zn2+solution wasnot reﬂecting the results obtained in the QCM experiments performed with the solution of the same composition. Exposing ZnO nanocrystal- lineﬁlms to solutions at comparable reaction times and consecutive rinsing did not lead to theformationofprecipitationﬁlms (seesupple-mentary information, Figure S2), which would indicate that their for- mation occurs at the interface due to the dissolution of ZnOnanocrystallineﬁlm andcomplexformation, and not due to theadsorp-tion ofaggregatesformed in the bulksolution.
WatercontactanglemeasurementshavebeenperformedonnanocrystallineZnO surfacesbeforeandafter adsorptionexperi-mentstoassessthetermsofsurfacehydrophobicityasanindicatorofﬁlmquality.Theas-preparednanocrystallineZnOﬁlmsurfacehas awater contact angleof 63°±2°, whichwasincreasedto 114±2°and110±1°afteradsorptionofODPAwithoutaddition ofZn2+ionsandwith the additionof 0.1 mMZn2+,respectively.WhentheZn2+concentrationintheODPAsolutionwasincreased to1.0mMZn2+,thewatercontactangleincreasedto128°±2°,in-dicating thepresenceofanODPAﬁlmwith higher degree oforganisation.
Taking all results into consideration, the following mechanism ofalkylphosphonicaciddepositiononnanocrystallineZnOﬁlms could be proposed. Whenalkylphosphonicacidmoleculesare brought into con- tactwiththe ZnO crystals, they start to promote Zn2+dissolutionat theliquid/metaloxideinterface.TheZn2+ions formcomplexeswith phos- phonic acid and form a precipitation layer on partially dissolved ZnO crystals. This process has a weak dependence on the concentration of the ODPA monomer in the solution. In a series of experiments (results not shown here) performed with different concentrations of ODPA(5mMto0.05mM),thedissolutionofZnOandtheformationofthepre-cipitationﬁlmwasobservedwithvaryingdegreesofseverity.Moreover,theadsorptiontimenecessaryfor thecompletionof theﬁlmformationprocess increased signiﬁcantly with the decrease in the ODPA concen- tration.Theresultspresentedhereindicatethattheformationofprecip-itationﬁlms could be prevented with the addition of appropriateamountsof Zn2+ions in thesolutionduring ODPAadsorption.
AppendixA.Supplementarydata
Supplementarydatatothisarticlecanbefoundonlineathttp://dx.doi.org/10.1016/j.colcom.2014.08.004.
References
1. A.Abdolmaleki,S.Mallakpour,S.Borandeh,Preparation,characterizationandsur-face morphology of novel optically active poly(ester-amide)/functionalized ZnObionanocompositesviaultrasonicationassistedprocess,Appl.Surf.Sci.257(2011)6725–6733.
2. Z. Chen, Y. Tang, L. Zhang, L. Luo, Electrodeposited nanoporous ZnOﬁlmsexhibitingenhanced performance in dye-sensitized solar cells, Electrochim. Acta 51 (2006)5870–5875.
3. LeGreene,M.Law,J.Goldberger,F.Kim,J.C.Johnson,Y.F.Zhang,R.J.Saykally,P.D.Yang, Low-temperature wafer-scale production of ZnO nanowire arrays, Angew.Chem. Int. Ed. 42 (2003)3031–3034.
4. J.J. Wu, C.H. Tseng, Photocatalytic properties of nc-Au/ZnO nanorod composites,Appl. Catal. B Environ. 66 (2006)51–57.
5. O. Ozcan, K. Pohl, P. Keil, G. Grundmeier, Effect of hydrogen and oxygen plasmatreatmentsontheelectricalandelectrochemicalpropertiesofzincoxidenanorodﬁlms on zinc substrates,Electrochem.Commun. 13 (2011)837–839.
6. O.Ozcan,K.Pohl,B.Ozkaya,G.Grundmeier,Molecularstudiesofadhesionandde-adhesion on ZnO nanorodﬁlm-covered metals, J.Adhes. 89 (2013) 128–139.
7. B.Baruwati,D.K.Kumar,S.V.Manorama,Hydrothermalsynthesisofhighlycrystal-lineZnOnanoparticles:acompetitivesensorforLPGandEtOH,SensorsActuatorsB Chem. 119 (2006)676–682.
8. T.Gao,T.H.Wang,Synthesisandpropertiesofmultipod-shapedZnOnanorodsforgas-sensorapplications,Appl.Phys.A:Mater.Sci.Process.80(2005)1451–1454.

14
A.Pomorskaetal./ColloidsandInterfaceScienceCommunications2(2014)11–14
1. T.Kong,Y.Chen,Y.P.Ye,K.Zhang,Z.X.Wang,X.P.Wang,AnamperometricglucosebiosensorbasedontheimmobilizationofglucoseoxidaseontheZnOnanotubes,SensorsActuatorsB Chem. 138 (2009)344–350.
2. P.I. Reyes, Z. Zhang, H. Chen, Z. Duan, J. Zhong, G. Saraf, Y. Lu, O. Taratula, E.Galoppini,N.N.Boustany,AZnOnanostructure-basedquartzcrystalmicrobalancedevice for biochemical sensing, IEEE Sensors J. 9-10 (2009)1302–1307.
3. A.Wei,X.W.Sun,J.X.Wang,Y.Lei,X.P.Cai,C.M.Li,Z.L.Dong,W.Huang,EnzymaticglucosebiosensorbasedonZnOnanorodarraygrownbyhydrothermaldecomposi-tion, Appl. Phys. Lett. 89 (2006)123902.
4. B. Zhang, T. Kong, W. Xu, R. Su, Y. Gao, G. Cheng, Surface functionalization of zincoxidebycarboxyalkylphosphonicacidself-assembledmonolayers,Langmuir26-6(2010)4514–4522.
5. M.Voigt,M.Klaumunzer,A.Ebel,F.Werner,G.Yang,R.Marczak,E.Spiecker,D.M.Guldi,A.Hirsch,W.Peukert,SurfacefunctionalizationofZnOnanorodswithC-60derivatives carrying phosphonic acid functionalities, J. Phys. Chem. C 115-13(2011)5561–5565.
6. M.Guo,P.Diao,S.Cai,HighlyhydrophilicandsuperhydrophobicZnOnanorodarray
ﬁlms, Thin Solid Films 515 (2007) 7162–7166.
1. J.Y.Dai,J.J.Cheng,J.Jin,Z.G.Li,J.Kong,S.P.Bi,Room-temperatureionicliquidasanewsolventtopreparehigh-qualitydodecanethiolself-assembledmonolayersonpolycrystalline gold, Electrochem. Commun. 10 (2008)587–591.
2. J.Y. Dai, Z.G. Li, J. Jin, J.J. Cheng, J. Kong, S.P. Bi, Study of the solvent effect on thequality of dodecanethiol self-assembled monolayers on polycrystalline gold, J.Electroanal. Chem. 624 (2008)315–322.
3. G.K.Jennings,J.C.Munro,T.H.Yong,P.E.Laibinis,Effectofchainlengthonthepro-tection of copper by n-alkanethiols, Langmuir 14-21 (1998)6130–6139.
1. E. Hoque, J.A. DeRose, P. Hoffmann, B. Bhushan, H.J. Mathieu, Alkylperﬂuorosilaneself-assembled monolayers on aluminum: a comparison with alkylphosphonateself-assembledmonolayers,J.Phys.Chem.C111(2007)3956–3962.
2. N.Adden,L.J.Gamble,D.G.Castner,A.Hoffmann,G.Gross,H.Menzel,Phosphonicacidmonolayersforbindingofbioactivemoleculestotitaniumsurfaces,Langmuir22 (2006)8197–8204.
3. W.Gao,L.Dickinson,C.Grozinger,F.G.Morin,L.Reven,Self-assembledmonolayersofalkylphosphonicacids on metal oxides, Langmuir 12-26 (1996)6429–6435.
4. K.Araki,K.Uezu,M.Goto,S.Furusaki,Bi-functionalorganophosphorusextractantsand computational modeling for copper(II) and zinc(II) extraction, Anal. Sci. 15(1999)651–656.
5. E.M.Wong,P.G.Hoertz,C.J.Liang,B.-M.Shi,G.J.Meyer,P.C.Searson,Inﬂuenceofor-ganic capping ligands on the growth kinetics of ZnO nanoparticles, Langmuir 17(2001)8362–8367.
6. L.E. Greene, M. Law, D.H. Tan, M. Montano, J. Goldberger, G. Somorjai, P. Yang,General route to vertical ZnO nanowire arrays using textured ZnO seeds, NanoLett. 5-7 (2005)1231–1236.
7. S.P.Garcia,S.Semancik,Controllingthemorphologyofzincoxidenanorodscrystal-lizedfromaqueoussolutions:theeffectofcrystalgrowthmodiﬁersonaspectratio,Chem. Mater. 19 (2007)4016–4022.
8. M. Giza, P. Thissen, G. Grundmeier, Adsorption kinetics of organophosphonicacidsonplasma-modiﬁedoxide-coveredaluminumsurfaces,Langmuir24(2008)8688–8694.