Catal Lett (2016) 146:1231–1241 DOI 10.1007/s10562-016-1748-z
Oxidative Dehydrogenation of Ethylbenzene OverPoly(furfuryl
alcohol)-Derived CMK-1 CarbonReplica
Sebastian Jarczewski1•Marek Drozdek1•Anna Wach1•Barbara Dudek1•
Piotr Kus´trowski1•Mirian Elizabeth Casco2•Francisco Rodr´ıguez-Reinoso2
Received: 25 March 2016 / Accepted: 6 April 2016 / Published online: 15 April 2016
©The Author(s) 2016. This article is published with open access at Springerlink.com
Abstract Poly(furfuryl alcohol) was introduced into a pore system of MCM-48 silica by the precipitation poly- condensation of furfuryl alcohol (FA). The complete filling of the pores without the deposition of significant amounts of polymer on the external surface of MCM-48 wasobtained at the FA/MCM-48 mass ratio close to 1.0. The final structure of carbon replica was formed by subsequent carbonization and extraction of SiO2with HF.The
carbonization temperature strongly influenced the surface composition of the formed carbon replicas. The highest catalytic activity in the oxidative dehydrogenation of ethylbenzene was observed for CMK-1 with the highest concentration of phenol and carbonyl groups, recognizedas activesitesofthestudiedreaction.
Graphical Abstract
ElectronicsupplementarymaterialTheonlineversionofthisarticle(doi:10.1007/s10562-016-1748-z)containssupplementarymaterial,whichisavailabletoauthorizedusers.
Keywords Ordered mesoporous carbons·Replication·
CMK-1·Oxidative dehydrogenation of ethylbenzene·
Styrene
&
Piotr Kus´trowskikustrows@chemia.uj.edu.pl
1 Introduction
1
Department of Chemical Technology, Faculty of Chemistry,JagiellonianUniversity,Ingardena3,30-060Krako´w,Poland
Laboratorio de Materiales Avanzados, Departamento deQu´ımicaInorga´nica,UniversidaddeAlicante,Apartado99,03080 Alicante, Spain
Porous carbon materials, especially activated carbons (ACs), offer a variety of prospective applications in catalysis, separation, purification or energy and gas storage [1–8], due to highly developed specific surface area,
2
13

1232
S. Jarczewski et al.
susceptibility to chemical modifications, availability of technologies of large-scale synthesis as well as environ- mentally friendly character. It was proved that in catalytic applications carbon materials can be used as effective supports of active phase. Moreover, unmodified carbons are active catalysts in many reactions involving oxygen- containing surface functionalities as active sites (e.g. oxidative dehydrogenation of ethylbenzene (ODH), dehy- dration of alcohols, SOxoxidation, NOxreduction) [9]. Recently, Yang et al. [10] have described a high catalytic activity of polyacrylamide-based cryogels in the transes- terification of fatty glyceride. Furthermore, carbon mate- rials appeared to be effective catalysts in the dehydrationof hemicellulosis sugars [11] as well as in the 1,2-dichlor- oethane (DCE) dechlorination [12]. However, the spatial structure of majority of investigated carbons consists mainly of disordered micropores, which may hinder internaldiffusionofreagentsduringcatalyticprocesses.
Many various carbon structures with an expanded pore system, including graphene-based materials [13] and nanofibers [14], were developed. Among them, ordered mesoporous carbons (OMCs) seem to be ideal candidates to overcome foregoing drawbacks of ACs. These materials exhibit a significant contribution of well-ordered meso- pores, which act as wider transport channels for reagents and reduce the diffusion limitations. The main concept ofsynthesis of OMCs is based on replication of structure of a soft or hard template using a carbon precursor [15]. Thesoft templating technique includes mixing of a carbon precursor and a pore forming agent (surfactant) to induce the self-assembly process of molecules into micelles gen- erating 3-D structures. Subsequently, polymerization of the carbon precursor is initialized, and the surfactant is elimi- nated from the obtained composite by carbonization. Unfortunately, the control of pore size, pore wall thickness and pore structure of OMCs produced by thesoft-tem- platingmethodisdifficult.Ontheotherhand,thesetextural parameters can be precisely controlled using the hard- templating route, but this approach requires a suit- able porous material (so called hard template) with a desired pore structure, which is usually synthesized in the first step. After filling the pore system of templatefollowed by carbonization of the formed composite, the template is removedandthecarbonreplicaisobtained.
The CMK-type materials (Carbon Mesostructured by KAIST), developed by Ryoo et al. [16], with various types of carbon mesoporous replicas (e.g. CMK-1, CMK-2, CMK-3 or CMK-6) synthesized using the silica template with the strictly defined pore structure (MCM-48, SBA-1, SBA-15 or SBA-16, respectively) are the most important family belonging to OMCs. The pore architecture of the silica template determines the spatial arrangement of final carbon material and the method of carbon precursor
deposition as well. Two methods of introduction of carbon precursor are usually used, i.e. infiltration the silica nano- pores with a solution of carbon precursor (i.e. sucrose, furfuryl alcohol or phenolic resin) at ambient temperature or chemical vapor deposition (CVD) performed at elevated temperatures [17].
The CMK-3 replica with hexagonal structure has been extensively studied in various applications which are typ- ical of ACs, whereas other CMK materials have been investigated significantly less often. It should however be believed that CMK-1 (described by Ryoo et al. [18]) canbe unappreciated since it exhibits higher specific surface area than CMK-3, which can increase a number of sitesexposedonthecarbonsurface.Moreover,Lez_an´skaetal.[19]showed that more acidic centers can be created on the surface of CMK-1 than CMK-3. The results of recent studies on CMK-1 confirm that this carbon replica is promising in some potential applications, e.g. in dye industry,gasseparationorhydrogenstorage[20–23].
In the presented work, the synthesis of CMK-1 carbon replicas by precipitation polycondensation of furfuryl alcohol (being the carbon precursor) in the pore system of MCM-48 silica, followed by carbonization of the resulting composite and SiO2extraction, was developed. The obtained materials were tested as catalysts of ODH, which involves carbonyl/quinone surface groups.
2 Experimental
2.1 Synthesis
For the MCM-48 synthesis, 32 mL of cetyltrimethylam- monium chloride solution (CTACl, 25 wt% in H2O, Aldrich) was dissolved in a mixture of 134 mL of distilled water, 210 mL of methyl alcohol (C99.8 %, Sigma- Aldrich) and 60 mL of 25 % ammonium hydroxide solu- tion (Sigma-Aldrich) under vigorous stirring (400 rpm) at room temperature in a round-bottom flask (500 mL). Subsequently, 18 mL of tetraethyl orthosilicate (TEOS, 98 %, Aldrich) was added dropwise (3 drops/s) and the mixture was stirred at room temperature for 2 h. The resulting solid product was filtered, washed with distilled water(800mL)anddriedat60°Covernight.Finally,the
material was calcined in air atmosphere at 550°C for 6 h
(at a heating rate of 1°C/min).
The prepared MCM-48 material was used as a hard template for the synthesis of CMK-1 replicas, using the modified procedure described by Niebrzydowska et al. [24]. A carbon precursor was deposited in the pores of MCM-48 by precipitation polycondensation of furfuryl alcohol (FA, 98 %, Aldrich) in an aqueous slurry of silica, catalyzed by HCl (35–38 %, Chempur). The intended PFA/
13

Oxidative Dehydrogenation of Ethylbenzene Over Poly(furfuryl alcohol)-Derived CMK-1 Carbon…
1233
MCM-48 mass ratio of 0.50–2.00 (with a step of 0.25) was controlled by an appropriate amount of FA. The molarratio of HCl/FA was kept constant at 6:1. In a typical procedure, 3 g of MCM-48 dried initially at 120°C for 1 h, was dispersed in a round-bottom flask (250 mL) containing a mixture of adequate amount of FA and water, to obtain a total mass of 100 g. The flask was equipped with a reflux condenser, placed onto a magnetic stirrer and agitated (400 rpm) at room temperature for 0.5 h. Then, the proper volume of HCl was added and the temperature was raised up to 100°C. The obtained slurry was stirred at this tem- perature for 6 h. The resulting PFA/MCM-48 composite was filtered, washed with distilled water and dried at room temperature overnight. Subsequently, the obtained material was carbonized in a tubular furnace at 650, 750, 850, 950 or 1050°C for 4 h (at a heating rate of 1°C/min) in an inert atmosphere (N2). Finally, the silica template was removed by a treatment with 5 % HF solution at room temperature for 1 h. The produced carbon replica was fil- tered, washed with distilled water and ethyl alcohol (96 %, Avantor) and dried at room temperature overnight.The procedure of silica dissolution was repeated once. The samples before and after carbonization at 850°C are denoted as PFA_x/MCM-48 and C_x/MCM-48, respec- tively, whereas CMK-1 replicas are marked asy_CMK- 1_x(wherexis the intended PFA/MCM-48 mass ratio andyis the temperature ofcarbonization).
pressure of 0.99. The mesopore volumes were calculated using the BJH model from the adsorption branch of the isotherm, whereas the micropore volumes were computed using the t-plot theory.
Thermogravimetric analyses (TG) were performed with a SDT Q600 thermobalance (TA Instruments) in flowing air (100 mL/min) from 30°C up to 1000°C (at a heating rate of 20°C/min).
The surface composition of samples was investigated with X-ray photoelectron spectroscopy (XPS) using a Prevac photoelectron spectrometer equipped with a hemi- spherical analyzer (VG SCIENTA R3000). The spectra were taken using a monochromatized aluminum source Al Ka (E=1486.6 eV). The base pressure in the analyticalchamberwas5910-9mbar.Thebindingenergyscalewas calibrated using the Au 4 f7/2line of a cleaned gold sample at 84.0 eV. The surface composition was analyzed taking into account the areas and binding energies of C 1 s and O 1 s core levels. The spectra were fitted using CasaXPS software.
Temperature-programmed desorption (TPD) was per- formed to determine the nature and total amount of oxy- gen-containing surface functionalities of CMK-1 carbon replicas. The experiments were carried out by heating 100 mg of sample placed in a U-shaped microreactor from ambienttemperatureupto1000°C(ataheatingrateof
10°C/min) under a helium flow (50 mL/min). Evolving
CO and CO2were analyzed quantitatively with an Omnistar Balzer MSC200 quadrupole massspectrometer
2.2 Characterization
after calibration based on calcium oxalate (CaC2O4·H2O)
Powder X-ray diffraction (XRD) measurements were per- formed on a Bruker D2 Phaser instrument using Cu Karadiation(k=1.54184A˚)andaLYNXEYEdetectorinthe2hrangefrom0.5to8.0°withastepof0.02°and1s
counting time per the step. The structure of MCM-48 and CMK-1 materials was also investigated with transmission electron microscopy (TEM). Prior to the experiment, the samples were deposited on a copper grid with a carbonfilm support. The images were collected with a JOEL JEM- 2010 microscope equipped with an Oxford Inca Energy TEM 100 detector and a Gatan Orius SC600 digital cam- era, operating at 200kV.
Nitrogen adsorption–desorption isotherms were mea-suredat-196°CusingaMicromeriticsASAP2020sorptometer. Prior to the measurement, a sample was degassedinvacuumat350°Cfor5h.Thespecificsurface areaswerecalculatedusingtheBrunauer–Emmett–Teller (BET)method.TheporesizedistributionsofPFA/MCM- 48compositesandCMK-1replicaswerecalculatedusing non-local density functional theory (NLDFT) and quen- ched solid density functional theory (QSDFT), respec- tively. The values of total pore volumes were obtained from the amount of adsorbed nitrogen at therelative
decomposition. The deconvolution of CO and CO2profiles was performed by using multiple Gaussian functions with non-linear optimization procedure based on the Leven- berg–Marquardt iteration algorithm.
2.3 Catalytic Tests
The CMK-1 carbon replicas were tested as catalysts in the oxidative dehydrogenation of ethylbenzene (EB) to styrene in the presence of oxygen at a molar ratio of O2:EB=1:1. The reaction was carried out in a packed bed flow microreactor with 50 mg of a sample placed onto a quartz wool plug. The temperature was measured with a ther- mocouple, protected by a quartz capillary inserted directly into a catalyst bed. The gaseous reactants were fed through mass flow controllers (Brooks 4800) at a total flow rate of 50 mL/min. EB vapor was introduced into the flow of He (49.6 mL/min)?O2(0.4 mL/min) mixture by passing it through a glass saturator filled with liquid EB and kept at 25°C. The products of the reaction were sampled with a pneumatic valve and transferred into a gas chromatograph system (Bruker 450-GC) via a heated line. The gas chro- matograph was equipped with three packed columns
13

1234
S. Jarczewski et al.
(Porapak Q, Molecular Sieve 5A and Chromosorb W-HP) connected with two flame ionization detectors (one ofthem directly connected to a catalytic methanizer) and one thermal conductivity detector. Prior to a catalytic run, a sample was outgassed at 200°C in flowing He (50 mL/ min) for 30 min. Subsequently, the temperature of catalyst was increased up to 350°C and dosing of reactants begun. After 15 min time-on-stream, the first sample of outlet stream was injected to GC and the analysis started. The chromatographic analyses were performed in 42 min intervals with a total time of 7 h. The catalyst performance was evaluated in terms of ethylbenzene conversion, yield of styrene and selectivity to particular products according to the followingequations:
XEB¼((FEB;0-FEB=(FEB;0x100%
(

Y¼F=F	x100%
i
i	EB;0
Si¼ ðYi=XEBÞx100%
where
XEB,
conversion of ethylbenzene;
FEB,0
andFEB,
molar flow rate of EB in the inlet and outlet streams;Yi, yield ofiproduct;Fi, molar flow rate of EB transformed intoiproduct,Si, selectivity ofiproduct.
Fig. 1 Efficiency of poly(furfuryl alcohol) deposition in the MCM- 48 poresystem
Toinvestigatetheseeffects,thelow-temperaturenitrogenadsorptionmeasurementswereperformedfortheneatMCM-48 and the C/MCM-48 materialsaftercarbonizationat 850°C. The collected isotherms are presented inFig.2a.AcharacteristicreversibleisothermoftypeIV,accordingtotheIUPACclassification,withsharpinflectionatrelativepressures between 0.15 and 0.35 due to thecapillarycon-densationwithinuniformmesopores,isobservedfortheMCM-48support[25,26].InthecaseoftheC/MCM-48composites,theshapesofisothermschangecontinuouslywith increasing the polymer to silica mass ratio,becauseofcarbonprecursorfillsgraduallytheporesystem.Anintro-ductionofhigheramountofPFAleadstothechangeinisotherm shape into type I (according to theIUPACclassi-fication),whichistypicalofmicroporousmaterials[26].Thefirstinflectionatlowrelativepressures(p/p0\0.1)becomessharperwiththeincreaseinamountofdepositedpolymerindicatingmoreuniformcharacterofmicroporesaswellasprogressiveblockingmesopores.Ascanbeseen,thedifference between the amount of adsorbed nitrogenfortheC_1.00/MCM-48	and	C_1.25/MCM-48	samples	isinsignificant. It is obvious that the carbonprecursorgradu-allyclogsthemesoporesofMCM-48withtheincreasingPFA/MCM-48massratiountiltheirtotalblockagefoundfortheC_1.25/MCM-48samplewiththerealPFA/SiO2of1.01.Theporesizedistributions(PSD)oftheMCM-48andC/MCM-48materialscalculatedusingtheNLDFTmodel
areshowninFig.2b.Asexpected,asystematicshiftofaverageporediameterisobservedfrom34A˚(formeso-
porous MCM-48) to lower values (for the C/MCM-48
3 Results and Discussion
3.1 Pore Filling in Mesoporous MCM-48
In order to determine the efficiency of alcohol) deposition in the MCM-48 pore
poly(furfurylsystem, ther-
mogravimetric measurements were performed. During the TG analysis, the introduced PFA was completely oxi- dized. Therefore, the determined mass of remaining sil- ica template allowed to calculate the contribution of organic part in the PFA/MCM-48 composites after sub- traction of mass loss attributed to desorption of physi- cally adsorbed water (observed below 200°C). The comparison between the intended and real PFA/MCM-48 mass ratios is presented in Fig.1. It should be noticed that the estimated efficiency of PFA precipitation is almost constant and equal to ca. 80 % for all synthesized samples. The lower PFA loading than theoretical can be assigned to the formation of PFA oligomers not attached to the silica surface, which were lost during filtration. This explanation was confirmed by yellowish color of the filtrate detected after the polycondensation process. It should be realized that the deposition of polymer in the silica pores was hindered by limited diffusion of the monomer and the catalyst in the highly complex gyroid- type pore structure of MCM-48. Thus, varying location of the formed polymer in the produced compositescan also beexpected.
13

Oxidative Dehydrogenation of Ethylbenzene Over Poly(furfuryl alcohol)-Derived CMK-1 Carbon…
1235
composites). Mesoporosity disappears entirely for the C_1.25/MCM-48 sample. Additionally, the samples con- taining PFA-derived carbon exhibit the presence of micropores, which are most likely formed inside thecarbon filler as well as between the carbon rods and silica walls due to the structure shrinkage undergoing during the car- bonization process[27].
The textural parameters, i.e. specific surface areas(SBET) and total pore volumes (Vtotal), are depicted in Fig.2c. It could be noticed that the gradual increase in the amount of PFA deposited in the pores of silica template results in the systematic decrease of SBETand Vtotal, from 1294 m2/gand
0.84 cm3/g for neat MCM-48, to 151 m2/g and 0.09 cm3/g for C_1.25/MCM-48, respectively. However, thedifference in the SBETand Vtotalvalues between the C_1.00/MCM-48 and C_1.25/MCM-48 samples is onlyslight.
Concluding, the specific shape of isotherms, pore diameters as well as textural parameters of C/SiO2com- posites clearly confirm that the complete filling of MCM- 48 pores with carbon precursor occurs at the real PFA/ MCM-48 mass ratio of about 1.0.
3.2 Influence of PFA/MCM-48 Mass Ratio
on Structural and Textural Properties of CMK- 1 Carbon Replica
After carbonization at 850°C and the removal of silica template with hydrofluoric acid, the resulting CMK-1 replicas were investigated in terms of their textural prop- erties.Theisothermsofnitrogenadsorptionrecordedforthe carbon replicas, shown in Fig.3a, are typical of a CMK-1 material, with a hysteresis loop above p/p0=0.4 [27]. As can be inferred from the relative position of isotherms, the volume of N2adsorbed increases constantly, achieving maximum for the CMK-1_1.25 sample. The higher PFA/ MCM-48 mass ratios result in a decrease of amount of N2adsorbed. The PSD calculated using the QSDFT model are presented in Fig.3b. Each sample exhibits three different kinds of pores with average diameters centered at about11,
17and34A˚.Thisclearlyconfirmsthattheobtained
materialshavemicro-mesoporousnature.Itshouldhowever be stressed that the presence of microporosity is typical of carbonized PFA [28,29]. Furthermore, the CMK-1_1.50, CMK-1_1.75 and CMK-1_2.00 samples show anadditional
typeofpores,withanaverageporediameterscloseto22A˚,
whichareabsentforthesamplesobtainedatthelowerPFA/SiO2mass ratios. It could be assumed that this porosity might originate from PFA deposited on the externalsurface ofMCM-48.
The total pore volumes and BET surface areas of the synthesized CMK-1 carbon replicas as a function of real
Fig. 2 Low-temperature N2adsorption isotherms (a), pore size distributions (b) and textural parameters [total pore volumes (Vtotal), specific surface areas (SBET)] as a function of real PFA/MCM-48 massratio(c)forMCM-48andthecarbon/silicacomposites
13

1236
S. Jarczewski et al.
bFig. 3 Low-temperature N2adsorption isotherms (a), pore size distributions (b) and textural parameters [total pore volumes (Vtotal), specific surface areas (SBET)] as a function of real PFA/MCM-48 mass ratio (c) for the carbon replicas carbonized at 850°C. The pore sizedistributioncurvesofCMK-1_0.50–2.00wereshiftedvertically
by0.04,0.08,0.12and0.16cm3/gA˚,respectively
PFA/MCM-48 mass ratio are shown in Fig.3C. SBETand
Vtotal
continuously increase with the raising amount of
carbon precursor and reach the maximum of 1730 m2/g (for CMK-1_1.25) and 1.06 cm3/g (for CMK_1.50), respectively. The higher polymer/silica mass ratios lead to a decrease in the value of foregoing parameters, finally to 1299 m2/g and 0.86 cm3/g for CMK-1_2.00, respectively. Thelattereffectcanbeattributedtotheadditionalamount
of carbon precursor deposited onto the external surface of MCM-48, which blocks pore system of formed replicaafter carbonization and silica removal. This is in agreement with the shape of CMK-1_2.00 isotherm, as described above. ThesametrendcanbeobservedfortheVtotalparameter.
The small-angle XRD patterns were collected forMCM- 48 and CMK-1 replicas carbonized at 850°C (cf. Fig. S1in Supporting Information and Fig.4, respectively). TheXRD pattern of MCM-48 reveals four well defined peaks typical of a gyroid-type structure, which can be indexed as (211), (220), (420) and (332) reflections in the cubicIa3dspace group [30,31]. The introduction of carbon precursor to the pore system, the subsequent carbonization and the silica removal resulted in an appearance of new diffraction lineat about 1.8°. This peak is not characteristic for theIa3dspace group. Thus, the synthesized CMK-1 materials can- notbedescribedasexactreplicasofMCM-48.Probably,
Fig. 4 Low-angle X-ray powder diffraction patterns collected for the CMK-1 carbon replicas carbonized at 850°C
13

Oxidative Dehydrogenation of Ethylbenzene Over Poly(furfuryl alcohol)-Derived CMK-1 Carbon…
1237
Fig. 5 TEM micrographs for a MCM-48 silica template and b CMK-1_1.25 carbon replica carbonized at 850°C
the structural transition to another cubic space group (I4132) occurred, in which the discussed (110) diffraction line appears at 1.77°[31]. Such rearrangement is possible by a slight displacement of two carbon rods relative toeach other without rotation along the (001) axis and keeping each rodrigidly.
The CMK-1_1.25 replica obtained at therealPFA/MCM-48 mass ratio of ca. 1.00, conclusively turnedouttohaveoptimaltexturalandstructuralparameters.WhenthePFA/MCM-48massratioislower,theamountofcarbonprecursorisinsufficienttofillcompletelytheporesystemof silica template. Consequently, the spatialstructureofcarbon replica is weak and has tendency to collapse.Ontheother hand, exceeding the optimalPFA/MCM-48massratio results in the formation of additionalPFAdepositedoutsidetheporesystemofsilicatemplate.Aftercar-bonization,itblockstheporesofproducedcarbonreplica.The TEM micrographs of neat MCM-48andCMK-1_1.25 carbonized at 850°C are demonstrated in Fig.5.Itcanbenoticedthatbothsamplesexhibitanuniformporedistribution and a regular arrangement ofmesopores[18,31]. Furthermore, the thin edges of CMK-1revealtheabsence of carbon deposited on the externalsurfaceofreplica particles [18]. This evidently confirmsthattheCMK-1_1.25 sample exhibits the properstructure, which
was expected to be synthesized.
according to the QSDFT model are presented in Fig.6B. All isotherms exhibit a similar shape with hysteresis loop above p/p0=0.4, which has been found previously for CMK-1_1.25 calcined at 850°C. Only isotherm of CMK- 1_1.25 calcined at the highest temperature shows clearly higher adsorption at low relative pressures, which suggests the presence of additional micropores. It should therefore be assumed that the carbonization temperature of 1050°C was high enough to generate significantly higher microp- orosity (cf. Table1). This effect is also confirmed by PSD (Fig.6B). For all samples three well resolved peaks assigned to the pores with diameters of about 11, 18 and
31A˚canbedistinguished.Nevertheless,inthecaseofthe
material calcined at 1050°C a considerably higher volume of micropores is observed.
The presence of oxygen-containing surface functionali- ties on the surface of CMK-1_1.25 replica carbonized at different temperatures was studied by temperature-pro- grammed desorption. The lines at m/z=28 and 44 allowed to observe decomposition of surface groups into CO and CO2, respectively. The obtained TPD profiles (cf. Fig. S2 in Supporting Information) give information on the type of these species and their relative content. Phenolsand carbonyl/quinone groups decompose forming CO at high temperatures, whereas CO2appears as a product of decomposition of carboxylic groups in the low-temperature range and/or anhydrides/lactones at higher temperatures [2,9,32–35]. Accordingly, in the case of CO evolution, two high-temperature peaks can be recognized in the TPD profiles, in the temperature ranges of 630–685 and 775–825°C, which can be assigned as phenol and carbonyl functional groups, respectively [2,9,32–35]. Furthermore, in the CO2profiles, three peaks can be distinguished in the temperature ranges of 260–285, 515–565 and 615–670°C correspondingtodecompositionofcarboxylic,anhydrides
3.3 Influence of Thermal Treatment Conditions
on Texture and Surface Composition of CMK-1 Carbon Replica
The nitrogen adsorption–desorption isotherms collected for the CMK-1_1.25 carbon replica carbonized at different temperatures (650, 750, 850, 950 or 1050°C) are shown in Fig.6A, whereas the corresponding PSD calculated
13

1238
S. Jarczewski et al.
calculated. The results of quantitative analysis of surface composition are summarized in Table2. It is obvious that the content of surface groups, which decompose with the formation of CO2, is significantly lower than those forming CO due to differences in their thermal stability. The ther- mal treatment at temperatures C650°C effectively elimi- nated less stable –COO– species. On the other hand, even so high carbonization temperatures influence the surface composition. It should be noticed that the concentration of carbonyl groups, considered as the active sites of ODH process, achieves the maximum after carbonization at 750°C.
The XPS measurements of CMK-1_1.25 provide a fur-
ther insight into distribution of oxygen-containing groups on the external surface of the materials calcined at different temperatures. The O 1 s and C 1 s high resolution XPS spectra are presented in Figure S3 in Supporting Informa- tion, whereas the determined contents of surface species are collected in Table3. The O 1 s core level spectrum reveals the existence of two main different oxygen species that can be interpreted as: (1) the double-bonded oxygen atoms in ketones, esters and acids at lower bindingenergies (530.6–531.1 eV), and (2) the single-bonded oxygen in alcohols, ethers, esters and acids at higher binding energies (532.7–533.2 eV) [36,37]. Additionally, the contribution from oxygen in adsorbed water is also considered in the fitting procedure. The presence of these groups was also confirmed by the C 1 s core level spectra. The main con- tribution to the C 1 s photoelectron spectra is an asym- metric peak with an exponential tail centeredat
284.4±0.1 eV. This main peak represents carbon atoms in graphitic and disordered carbon species (C=Csp2and C–Csp3) [38]. The polyaromatic character of carbon replicas was furthermore confirmed by the presence of signal above 290.0 eV, which corresponds to shake-up satellite due to p–p* transitions in aromatic rings. Inaddition, the components due to oxidized carbon species were identified at 286.3 (±0.1), 287.4 (±0.1) and 288.5 (±0.1) eV, which can be assigned to C–OH/C–O–C, C=O and COOH, respectively [33,37].
The XPS analysis reveals the influence of carbonization temperature on the composition of uppermost, superficial surface layers. The data presented in Table3confirm the dominant role of phenol and carbonyl groups among the
Fig. 6
Low-temperature N2adsorption isotherms (a) and pore size
distributions (b) for the CMK-1_1.25 replicas carbonized at different temperatures
and lactones, respectively. To estimate the content of each
type of surface groups, the CO and CO2profiles
werewere
deconvoluted and the areas
of particular peaks
Table 1 Textural parameters of the CMK-1_1.25 replicas carbonized at different temperatures
SBET(m2/g)
Vmicro(cm3/g)
Vmeso(cm3/g)
Vtotal(cm3/g)
Sample

650_CMK-1_1.25
750_CMK-1_1.25
850_CMK-1_1.25
950_CMK-1_1.25
1050_CMK-1_1.25
1633
1653
1617
1635
1861
0.15
0.14
0.22
0.21
0.33
0.65
0.63
0.53
0.53
0.50
1.06
1.05
0.98
0.98
1.07
13

Oxidative Dehydrogenation of Ethylbenzene Over Poly(furfuryl alcohol)-Derived CMK-1 Carbon…
1239
Table 2 Temperatures of maxima of deconvoluted TPD profiles (TM) and the amounts of identified oxygen-containing surface groups (A) for the CMK-1_1.25 replicas carbonized at different temperatures
Sample
CO
CO2

Phenol
Carbonyl/quinones
Carboxylic
Anhydride
Lactone
Ta
Ab
Ta
Ab
Ta
Ab
Ta
Ab
Ta
Ab
M
M
M
M
M
650_CMK-1_1.25
750_CMK-1_1.25
850_CMK-1_1.25
950_CMK-1_1.25
1050_CMK-1_1.25
630
631
663
686
671
546
500
317
320
141
775
791
803
825
814
259
281
258
245
158
277
285
270
283
260
25
35
26
29
31
517
554
563
525
528
24
30
11
14
12
617
671
671
670
657
28
14
7
12
8
Temperature of the peak maximum (°C)
Amount of particular surface oxygen functional group (lmol/g)
a
b
Table 3 Surface composition of CMK-1_1.25 carbonized at different temperatures determined by XPS
Sample
Atomic concentration (%)

Oxygen
Carbon
C=Csp2, C–Csp3
C=O
C–O
C–OH, ethers, lactones
C=O
COOH/COOR
650_CMK-1_1.25
750_CMK-1_1.25
850_CMK-1_1.25
950_CMK-1_1.25
1050_CMK-1_1.25
0.72
2.41
2.61
1.45
0.67
2.68
2.91
2.73
2.39
2.28
80.72
75.25
76.74
77.67
78.04
2.56
3.53
3.06
2.71
2.54
0.51
2.10
2.33
1.19
0.45
0.21
0.31
0.28
0.26
0.22
functionalities present on the sample surface. This method detected the highest concentration of carbonyl moieties for the CMK-1_1.25 replica thermally treated at 850°C.
molecule. Finally, the formed hydroquinone groups are re- oxidized by oxygen with H2O evolution [9,35,39–42].
It is observed that over each studied sample theEBconversion decreases exponentially with the reaction time reaching a steady-state after ca. 6 h. The catalyst deacti- vation can be associated with the accumulation of car- bonaceous deposit. However, the coke plays a double role in the ODH catalyst. Firstly, it clogs the pores and limits the accessibility of reactants to the active sites. Secondly, the coke layer alters the chemical composition of the sur- face [35,40–42]. Those effects were previously observed in the ODH reaction over the acidic catalysts (such asSiO2, Al2O3) [42,43] and various carbon materials (ACs, multi- wallcarbonnanotubes,OMCs)[24,37,41,44].
Figure8presents the conversions of ethylbenzene and selectivity to styrene calculated after 6 h time-on-stream. The similar values of catalytic parameters suggest that the rate of coke deposition is very close, regardless on the surface composition of CMK-1 carbon replica. Neverthe- less, the material carbonized at 850°C exhibits the highest EB conversion. We have compared the activity and selectivity of this catalyst to the previously tested CMK-3 synthesized by the analogous method and carbonized at the same temperature, described in Ref. [24]. As is shown in Fig.8, CMK-1 gives slightly higher conversion thanCMK- 3 after 6 h on-stream time. However, the difference in the selectivitytostyreneismuchmoresignificant(98.4%for
3.4 Catalytic Activity of CMK-1 Carbon Replicas in Oxidative Dehydrogenation ofEthylbenzene
The CMK-1_1.25 carbon replicas carbonized at various temperatures were tested as catalysts of the oxidative dehydrogenation of ethylbenzene (EB) at 350°C and the EB/O2molar ratio of 1.0. The observed variations in the EB conversion and selectivity to styrene versus time-on- stream are shown in Fig.7. The initial activity of CMK- 1_1.25 is clearly affected by the carbonization temperature and correlates with the content of carbonyl/quinone groups determined by TPD and XPS. The highest conversion of ethylbenzene (30.2 %) is achieved over the sample car- bonized at 750°C with the highest concentration of these functional groups. On the other hand, the CMK-1_1.25 sample thermally treated at 1050°C, containing the lowest amount of carbonyl/quinone groups, shows much lowerEB conversion (19.4 %) than the other replicas, proving the strong influence of the surface composition on the catalytic performance. These results are consistent with the com- monly accepted ODH mechanism, which involves a redox cycle whereby an ethylbenzene molecule reacts with two adjacentcarbonyl/quinonegroupsandproducesastyrene
13

1240
S. Jarczewski et al.
Fig. 7
Conversion of ethylbenzene (a) and selectivity to styrene
Fig. 8 Conversion of ethylbenzene (a) and selectivity to styrene
(b) after 6 h time-on-stream for the CMK-1_1.25 replicas carbonized at different temperatures compared to the catalytic performance of CMK-3 sample (patterned columns) carbonized at 850°C [24]
(b) versus time on stream for the CMK-1_1.25 replicas carbonized at different temperatures
4 Conclusions
CMK-1 vs. 95.9 % for CMK-3). It should be kept in mind that selectivity to COxis inversely coupled to styrene at negligible selectivity to benzene and toluene [45]. More- over, it was postulated that the carbonaceous deposit is created by the styrene molecules [41,43]. It might bestated that the efficiency of the coke deposition affecting the styrene selectivity, depends on the time, in which the styrene molecules stay within the pores of carbon replica. This is due to a higher probability of styrene polymeriza- tion with a prolonged residence time. Taking into account the length of channels in the CMK-1 and CMK-3materials, the shorter residence time can be expected in the case of CMK-1 with the regular pore structure. The straight and long pores of CMK-3 cause the diffusion limitations and favor the coking process lowering the selectivity tostyrene.
Poly(furfuryl alcohol) was successfully deposited inthe pore system of regularly ordered MCM-48 mesoporous silica by the precipitation polymerization in the presence of HCl. At the real PFA/MCM-48 mass ratio of about 1.0, complete filling of mesopores by the formed polymer was observed. Carbonization of the obtained composites and the removal of SiO2resulted in the exposition of structure of CMK-1 carbon replica. It was shown that the pore structure and surface composition of this material depen- ded on the temperature used during carbonization. The increase in this temperature above 1000°C favored the formation of additional microporosity in the PFA-derived mesoporous carbon. On the other hand, theelevated
13

Oxidative Dehydrogenation of Ethylbenzene Over Poly(furfuryl alcohol)-Derived CMK-1 Carbon…
1241
temperatures caused the elimination of oxygen-containing functionalities present on the surface of replica. The TPDmeasurements showed that the highest concentration ofsurface phenol and carbonyl groups was achieved after thethermal treatment at 750°C. The carbon catalyst car-bonized at this temperature was the most active in theoxidative dehydrogenation of ethylbenzene to styrene aswell. This observation confirmed the catalytic role of C=O species as active centers in the ODH process. Furthermore, CMK-1 showed the slightly higher EB conversion and thesignificantly higher selectivity to styrene compared to CMK-3, described in the literature. The latter effect can beattributed to the better accessibility of active sites located within the regular pore structure with shorter transportchannels than in long, straight pores of hexagonallyorderedCMK-3.
1. Hajjar Z, Kazemeini M, Rashidi A, Bazmi M (2015) Catal Lett 145:1660
2. Cherkasov N, Savilov SV, Ivanov AS, Egorov AV, Lunin VV, Ibhadon AO (2014) Appl SurfSci 308:388
3. ZubizarretaL,IserteR,LloveraP,Gil-Agust´ıM(2011)Micro-
porous Mesoporous Mater 143:30
1. RyooR,JooSH,KrukM,JaroniecM(2001)AdvMater13:677
2. FuertesAB,NevskaiaDM(2003)JMaterChem13:1843
3. RyooR,JooSH,JunS(1999)JPhysChemB103:7743
4. Lez_an´skaM,PietrzykP,DudekA,WłochJ(2015)MaterChemPhys149–150:539
5. AnbiaM,GhaffariA(2012)IntJEng(TransBAppl)25:259
6. Ghani K, Kiomarsipour N, Jaberi H (2015) Dyes Pigments 122:126
7. PengX,CaoD,ZhaoJ(2009)SepPurifTechnol68:50
8. Jua´rezJM,Go´mezMB,AnunziataOA(2015)IntJEnergyRes39:941
9. Niebrzydowska P, Janus R,Kus´trowskiP, Jarczewski S, Wach A, Silvestre-Albero AM,Rodr´ıguez-ReinosoF (2013) Carbon 64:252
10. XuJ, Luan Z, He H, Zhou W, Kevan L (1998) Chem Mater 10:3690
11. SingKSW, Everett DH, Haul RAW, Moscou L, Pierotti RA,Rouque´rolJ,SiemieniewskaT(1985)PureApplChem57(4):603
12. KrukM, Jaroniec M, Ryoo R, Joo SH (2000) J Phys Chem B104:7960
13. MariwalaRK,FoleyHC(1994)IndEngChemRes33:607
14. BurketCL, Rajagopalan R, Marencic AP, Dronvajjala K, Foley HC (2006) Carbon44:2957
15. KimS, Marand E, Ida J, Guliants VV (2006) Chem Mater 18:1149
16. KanedaM, Tsubakiyama T, Carlsson A, Sakamoto Y, Ohsuna T, TerasakiO,JooSH,RyooR(2002)JPhysChemB106:1256
17. La´zaroMJ,CalvilloL,Bordeje´EG,MolinerR,JuanR,RuizCR(2007) Microporous Mesoporous Mater103:158
18. Zhou J-H, Sui Z-J, Zhu J, Li P, Chen D, Dai Y-C, Yuan W-K (2007) Carbon45:785
19. Szyman´skiGS,Karpin´skiZ,BiniakS,S´wia˛tkowskiA(2002)Carbon40:2627
20. FigueiredoJL,PereiraMFR(2010)CatalToday150:2
21. OkpalugoTIT, Papakonstantinou P, Murphy H, McLaughlin J, Brown NMD (2005) Carbon43:153
22. DarmstadtaH, Roy C, Kaliaguine S, Choi SJ, Ryoo R (2002)Carbon40:2673
23. Estrade-SzwarckopfH (2004) Carbon42:1713
24. EmigG,HofmannH(1983)JCatal84:15
25. PereiraMFR,O´rfa˜oJJM,FigueiredoJL(1999)ApplCatalA184:153
26. PereiraMFR,O´rfa˜oJJM,FigueiredoJL(2001)ApplCatalA218:307
27. CavaniF,Trifiro`F(1995)ApplCatalA133:219
28. CadusLE, Arrua LA, Gorriz OF, Rivarola JB (1988) Ind EngChem Res27:2241
29. PereiraMFR,FigueiredoJL,O´rfa˜oJJM,SerpP,KalckP,KihnY
(2004) Carbon 42:2807
Zarubina V, Talebi H, Nederlof C, Kapteijn F, Makkee M,Melia´n-CabreraI(2014)Carbon77:329
Acknowledgments This work was supported by the National Sci- ence Centre under the Grant No. 2013/09/B/ST5/03419. The research was carried out with the equipment purchased thanks to the financial support of the European Regional Development Fund in the frame- work of the Polish Innovation Economy Operational Program (con- tract No.POIG.02.01.00-12-023/08).
Open Access This article is distributed under the terms of the Creative Commons Attribution 4.0 International License (http://creativecommons.org/licenses/by/4.0/), which permits unrestricted use, distribution, and reproduction in any medium, provided you give appropriate credit to the original author(s) and the source, provide a link to the Creative Commons license, and indicate if changes were made.
References
1. Rodriguez-Reinoso F (1988) Carbon36:159
2. FigueiredoJL,PereiraMFR,FreitasMMA,O´rfa˜oJJM(1999)Carbon37:1379
3. Yong Z, Mata V, Rodrigues AE (2002) Sep Purif Technol26:195
4. YangH,XuZ,FanM,GuptaR,SlimaneRB,BlandAE,WrightI (2008) J Environ Sci20:14
5. Xu W-C, Takahashi K, Matsuo Y, Hattori Y, Kumagai M, Ish- iyama S, Kaneko K, Iijima S (2007) Int J HydrogenEnergy 32:2504
6. JinH,LeeYS,HongI(2007)CatalToday120:399
7. SircarS,GoldenTC,RaoMB(1996)Carbon34:1
8. Gamby J, Taberna PL, Simon P, Fauvarque JF, ChesneauM (2001) J Power Sources101:109
9. Serp P, Figueiredo JL (2009) Carbon materials for catalysis. Wiley, NewJersey
10. Yang C, Liu GF, Zhou XL, Liu YR, Wang J, Tian LL, Hu XY,Wang YY (2015) Catal Lett145:1778
11. SairanenE,KarinenR,LehtonenJ(2014)CatalLett144:1839
12. Tveritinova EA, Zhitnev YN, Kulakova II, CherkasovN, Maslakov KI, Nesterova EA, Ivanova AS, Savilova SV, Lunin VV (2015) Appl Surf Sci355:74
13