JElectroceram(2014)32:92–101DOI10.1007/s10832-013-9865-1
Effect of cobalt doping on the dielectric response of Ba0.95Pb0.05TiO3ceramics
E. Markiewicz&R. Bujakiewicz-Korońska&D. Majda&
L. Vasylechko&A. Kalvane&M. Matczak
Received:15January2013/Accepted:9September2013/Publishedonline:27September2013
#The Author(s) 2013. This article is published with open access at Springerlink.com
Abstract Dielectric response of
Ba0.95Pb0.05TiO3
ceramics
oforderingofpolar defectsinthe hostlatticeofBa0.95Pb0.05TiO3inaformpolar nanoregions.
doped with0.1 and1wt.%ofCo2O3,synthesizedbyconven-tionalhigh-temperaturemethod,wasstudiedinwidetemperatureandfrequency range.Thetemperature dependencesofthe realandtheimaginarypartsofdielectricpermittivityoftheceramicswerecomparedwith thoseofBaTiO3andBa0.95Pb0.05TiO3.The additionofCo3+ionsresultsinabroadeningofdielectricanom-aliesrelatedtothetransitiontoparaelectriccubic phase, andthe structuraltransitionbetweenthetetragonalandtheorthorhombicphases.Atlowtemperatures (125–200K)thedielectricabsorp-tionofCo-dopedBa0.95Pb0.05TiO3ceramicswasfoundtoexhibit relaxor-likeproperties.Thedielectricresponsehasbeenfoundto containthecontributionscharacteristicoffluctuationsofthepolarnanoregionboundariesandreorientationsofthedipolemoments betweenalloweddirectionsinthenanoregionsintherhombohe-dralandtheorthorhombic phases.Thebehavior speaksinfavor
E.Markiewicz(*):M.Matczak
Keywords Ba0.95Pb0.05TiO3.Co-doping.Dielectric properties.Deviation from the Curie-Weiss law
1 Introduction
BaTiO3(BT) is a classic ferroelectric which has foundwide application in the electronicindustry.BT ceramics is com- monly used in ceramic capacitors, piezoelectric sensors or actuators as well as resistive switching elements [1–3]. The compoundcanexistinfourphaseswithcubic(above398K), tetragonal(between398and281K),orthorhombic(between 281 and 202 K), and rhombohedral (below 202 K) crystal structure[4,5].Allofthephases,exceptthecubicone,exhibit ferroelectricproperties.
ThestructureandthedielectricpropertiesofBThavebeen extensively studied for more than half a century in order to increasethedielectricpermittivityandtosuppressthelosses [6,7].Nowadaystheresearchconcentratedontemperature–stable dielectrics are intensely developed [8]. Pure BT is characterized by large variations in dielectric permittivity anddielectriclossesrelatedtothestructuralphasetransitions. Inordertoavoidthesedisadvantages,dopingofpureceramics
InstituteofMolecularPhysics,PolishAcademyofScience,
Smoluchowskiego17,60-179Poznan,Poland e-mail:ewamar@ifmpan.poznan.pl
R. Bujakiewicz-Korońska
InstituteofPhysics,PedagogicalUniversity,Podchorążych2, 30-084Krakow,Poland
D. Majda
DepartmentofChemistry,JagiellonianUniversity,Ingardena3, 30-060Krakow,Poland
isused.BTisknowntoformsolidsolutionswithPbTiO(PT)
3
andanupwardshiftofthetemperatureofthetetragonal-cubic phasetransitionisobservedwithanincreaseofPbcontentin(1−x)BaTiO3−xPbTiO3solidsolutions[9–13].XAFSstud- ies by Lebedev at al. [13] indicated a displacement of Pb atomsfromtheAlatticesiteintheABO3perovskitestructure by~0.15Åandastrongdistortionoftheoxygenenvironment as the main factors responsible for the appearance of ferro- electricityinthetemperaturerangeabove~400K,thatistheCuriepoint ofpureBaTiO3[14–17]. Accordingtothe
L. Vasylechko
LvivPolytechnicNationalUniversity,12Bandera,79013Lviv,Ukraine
A. Kalvane
InstituteofSolidStatePhysics,UniversityofLatvia,Kengeraga8,LV-1063Riga,Latvia
M. MatczakNanoBiomedicalCentre,AdamMickiewiczUniversity,Umultowska 85, 61-614 Poznan,Poland
JECR SPECIAL ISSUE ON ELECTRO-CHEMO-MECHANICS

JElectroceram(2014)32:92–101
93
literature data [4] the temperatures of the transitions from tetragonaltoorthorombicandfromorthorhombictorhombo- hedral phases are lowered due to an addition of the Pb ions resulting in a broadening of the dielectric anomaly in the vicinity of roomtemperature.
DielectricpropertiesoftheceramicsbelongingtotheBaTiO3familycanbeinfluencedbydoping withthetransition–metalions.Ithasbeenfoundthationswiththevalencessmallerthan4substitutingtheTisitesexhibit acceptor characterwithchargedeficiencycompensatedbydoublyionizedoxygenvacancies[1,18].Amongthe3delementsCoisknowntoinfluencetheelasticand thedielectric propertiesoftheBaTiO3—based ceramics[2,19,20].Theadditionof Codopantup to1at.% resultsinan attenuationofmechanicallossesandasmoothingoftheelasticmodulus anomaly[2].Thedecreaseofmechanical lossesintheorthorhombicphaseisassociatedwiththefixingofthedomainwallpositionsbyCo3+acceptorions.Dielectricmeasurementby
H. J.HagemannandH.Ihrig[1]showedtheloweringoftheCurie point withthecontentof Codopantsup to2mol%.
The aimofthis paperistocharacterizetheeffectofCo—
families.Therelaxor-likebehaviorischaracterizedbybroadand highly dispersive dielectric anomaly[22–24].
Here we present the results of detailed studies of the di-
electric response of Co2O3doped
Ba0.95Pb0.05
ceramics to
searchforaninfluenceofintroduceddefectsontheequilibri- umbetweentheshort—andthelongrangeinteractionsinthe hostlattice.ThematerialwascharacterizedbyX-raydiffrac-tion(XRD)anddifferentialscanningcalorimetry(DSC).
2 Experimental
2.1Preparationofthesamples
BT—basedceramicswith5at.%ofPband0.1wt.%aswellas1wt.%ofCo2O3were preparedbystandardhightemperaturedrysintering method. ChemicalsfromAldrich:Co2O3(purity99.5%),BaCO3(99.5%),PbO(99.0%)andTiO2(99.5%)
wereused.TheBaCO3andTiO2powderwereweighedinaccordancetochemicalformulastoichiometrytoobtainBaTiO3ceramics.The BPT andBPTC ceramics were also preparedinaccordancetothepresumednominalcompositions.Thecompo-nentsweremixedinethanolandhomogenizedin anagateball-millfor24h.Afterdryingat400K,theywerecalcinedfor2hatthetemperatureof1,493K.Thenthecalcined powderswere grinded,pressed underthepressureof 15MPaatroomtemper-atureinformofpelletsindiameterof8mm,andsinteredfor2hat1,593K,atambientair.Thesampleswerecooledintheoven fromsintering temperaturetoroomtemperaturefor6h.EDX(Bruker-Quantax)studiesoffracturedBPTCsamplesshowthatthePbamountliesintherangefrom(5.38±0.22)to(7.79±0.28)wt.%.Thesamplesinformofdiscs,thicknessd=1mmanddiameterϕ=8mm,werecutofffordielectric measurements.Thediscs werecoveredwith gold sputteredelectrodes.
doping on the dielectric response of
Ba0.95Pb0.05TiO3
solid
solutionwith very lowtetragonality (1-c/a)andtocomparethe response with those of the undoped ceramics and theBaTiO3ceramics.Weexploretheimpactofdopingamaterialtomodifytheelectrical properties,i.e. therelationship betweenthechemicalandelectrical properties.Thisrelationshipcanbe eitherinagoodagreementwithbeneficial mechanical proper-ties as pointed out in [2] or it can be coupled with lowerpiezoelectricactivity[21].Thestudyofadjustingagivenprop-ertycanbeeasyadoptedtothecontroloftheanotherone.BT—basedceramicswith5 %PTand 0.1%aswellas1 %Co2O3dopingcanbeveryinterestingfromtheapplicationpointofviewbecauseoftheabilityofaflatteningthedielectric permit- tivity–temperaturecharacteristicbytheCoionsandashiftofthephasetransition temperaturesby the Pbdopants.Co3+acceptorions areincorporatedinto theTi4+-latticesitebecauseoftheir similarionic radii andoxygen vacanciesaregeneratedinordertocompensatethevalence.Theresultant acceptor–oxygen va-cancydipolesinhighlypolarizablelatticecanformeitherpolar nanoregions(PNRs)likeinferroelectricrelaxors[22–24]orcanresultin aninternalbias whichisformally equivalenttothe energy differenceofthedipolar defects betweentheaccessible directionsofthespontaneouspolarizationandaffectsthedielec-tricresponse [25–27].Duetohighpolarizabilityofthe ABO3latticethedipolar defects polarizetheneighboringpartofthelattice forming the polar nanoregions the size of which isdeterminedbytemperature–dependent correlation lengthofthe host. Forlowdefect concentrationeach polarnanoregioncanbetreatedasanoninteractingpolarobjectcharacterizedbyasinglerelaxationtime.AthigherdefectconcentrationsthePNRscaninteract leadingto more complexrelaxational behaviorapparentin socalled ferroelectric relaxorsas LasubstitutedPbZr1-xTixO3familyorPbMg1/3Nb2/3O3andPbSc1/2Nb1/2O3
2.2 XRDstudies
X-raypowderdiffractionstudiesoftheBa0.95Pb0.05TiO3andBa0.95Pb0.05TiO3+0.1%Co2O3ceramics were performed on thelaboratoryHuberimagingplateGuiniercameraG670withCuKα1radiation.ThecrystalstructureofBa0.95Pb0.05TiO3+0.1%Co2O3andBa0.95Pb0.05TiO3was determined from high- resolutionpowderdiffractionwithsynchrotronradiationinthe temperaturerange298–1,173K.Correspondinginsituhigh-temperaturediffractionexperimentswereperformedwith powder diffractometer at the B2 beamline ofsynchrotron laboratoryHASYLAB/DESY[28].TheprogrampackageWinCSD[29]wasusedinallcrystallographiccalculations.
2.3 DSCmeasurements
DSCmeasurementswerecarriedoutusingaDSC822eMettlerToledoapparatus,equippedwithliquidnitrogencoolingoption

94
JElectroceram(2014)32:92–101
Fig. 1 X-ray synchrotronpowder diffractionpatterns ofBa0.95Pb0.05TiO3(a)andBa0.95Pb0.05TiO3:0.1%Co2O3(b);λ=0.53827 Å atRT.
Experimental(dots) and calculated patterns,differenceprofiles and positions of thediffractionmaxima are given
(Cryofab).Thesampleofstudied materialwashermetically sealedin analuminum crucibleandmeasuredintemperaturerangefrom123Kto723Kataheatingrateof10K/min.Theemptypan was usedas areference sample.Theexperimentswererepeated twicetoconfirmtheresults.
andplacedintoacryostat.Themeasurementswereperformedinthetemperaturerange from 125K to525Konheatingatarateof1K/min.Thefrequency variedfrom1Hz to1MHzattheoscillation voltageof1V.Themeasured dielectric permit- tivitydata werecollectedandevaluatedbyWinDETAimped-anceanalysis softwareandaWinFitV3.2.program.
2.4Dielectricmeasurements
DielectricresponseoftheceramicsampleswasstudiedusinganAlpha-AHighPerformance Frequency Analyzer (NovocontrolGmbH)combinedwithQuatroCryosystemforthetemperature control.Thesamplewith goldsputtered electrodeswasfixed betweentwoadditional external electrodesin asampleholder
3Resultsanddiscussion
X-ray powder diffraction studies of the BPT and BPTC specimens at RT revealed tetragonal perovskite structure, similar to that of pure BT. Figure1shows the X-ray

JElectroceram(2014)32:92–101
95
Table 1 Crystallographic data for Ba0.95Pb0.05TiO3:0.1%Co2O3
andBa0.95Pb0.05TiO3atRT(space groupP4mm)
B	a,Å2
Atoms,sites
x
y
z
B
B
B
B,B	B
iso/eq
11
22
33
12 13, 23
Ba0.95Pb0.05TiO3:Co;a=3.99248(4) Å,c=4.03373(6) Å;RI=0.064,RP=0.113
Ba/Pb,1aTi/Co,1bO1,1b
O2, 2c
0
1/2
1/2
1/2
0
1/2
1/2
0
0.0001(6)
0.4884(7)
−0.019(2)
0.512(2)
0.751(4)
0.75(1)
0.83(6)
0.85(5)
0.735(5)
0.77(1)
0.90(10)
0.94(10)
B11B11B110.74(7)
0.783(9)
0.70(3)
0.69(13)
0.89(8)
0
0
0
0
Ba0.95Pb0.05TiO3;a=3.98898(9) Å,c=4.0380(1) Å;RI=0.068,RP=0.131
Ba/Pb, 1aTi, 1b
O1, 1b
0
1/2
1/2
0
1/2
1/2
0.0001(9)
0.4848(9)
−0.014(4)
0.756(8)
0.68(4)
0.75(14)
0.71(1)
0.73(2)
0.83(13)
B11B11
B11
0.84(2)
0.57(12)
0.6(4)
0
0
0
aBiso/eq=1/3[B11(a*)2a2+…2B23b*c*bccosa];T=exp[−1/4(B11(a*)2h2+…2B23b*c*
k l)]
O2,2c	1/2	0	0.518(2)	0.8(2)
1.4(2)	0.4(1)	0.7(4)	0

synchrotron powder diffraction patterns and the results of full profile Rietveld refinement obtained for both speci- mens. The final values of structural parameters are presented in Table1. Besides the lattice parameters, the atomic coordinates and anisotropic displacement parame- ters of atoms were refined.
Examinationofdiffraction patternsof BPTC and BPTcol- lectedattheelevatedtemperaturesshowsthattetragonaldefor- mation decreaseswithincreasing temperatureandcompletely vanishesatthetemperatures higherthan 453Kand 473KforBPTC andBPT,respectively (Fig.2). Thepatterns collected abovethistemperatureshow purecubic perovskite structure.Accordingly,crystal structure parametersofthetetragonal and cubicphasesofbothsampleshavebeenrefinedinspacegroupsP4mmandPm3m,respectively.Detailed examinationofthe diffraction patternsofBPTCcollectedinthevicinitiesofthe transitiontemperaturerevealedacoexistenceofbothtetragonalandcubicphasesinthetemperaturerange383K–423K(insetinFig.2),which provesthe1st-order discontinuouscharacter
ofthephase transitioninBPTC. Similar behaviourwasalso observedfor the BPTcrystal.
Simultaneoustwo-phaseRietveldrefinementperformedin space groupsP4mm andPm3mconfirms a coexistence of tetragonalandcubicperovskitephasesinthevicinitiesofthe transition temperatures. According to the data obtained, the amountofthetetragonalphaseinBPTCdecreasesfrom
90.0wt.%at383Kto20.5wt.%at423K,whereasthecontent of the cubic phase simultaneouslyincreases.
Figure3demonstrates the change in relative amounts of bothperovskitephasesinBPTCandBPTatthephasetransi- tions. From these plots the temperatures of the phasetransi- tions(thetemperaturesatwhichtheamountsoftetragonaland cubicphasesareequal)canbeestimatedas410Kand442K,respectively.
Temperaturedependenceofthelatticeparametersandcell volumesoftetragonalandcubicmodificationsofBPTCand BPTillustratingthefirst-orderstructuralphasetransitionare presented in Fig.4. The microstructural parameters ofBPT
Fig. 2Fragmentsofdiffractionpatterns collected in situ in thetemperaturerange 343–473 K withthetemperaturestepof10K (from thebottomto thetop)illustratingthe structural phase transition in BPTC (0.1%)

96
JElectroceram(2014)32:92–101
(a)
(a)
(b)
Fig. 4Temperaturedependences of the lattice parameters and cell vol- umes of tetragonal and cubic structures of BPTC (0.1 %)(a)and BPT(b).The areas ofcoexistenceof both perovskite phases aredashed
Fig. 3
Refinedvaluesoftheamountoftetragonalandcubicperovskite
phasesinBPTC(0.1%)(a)andBPT(b)inthetemperaturerangeofthe
phasetransitions
andBPTCsamples(averagegrainsizeDaveandmicrostrains parameters<ε>=<Δd>/d)wereobtainedfromtheanalysisof the broadening of X-ray powder diffraction maxima byWilliamson-Hallanalysis,whichallowstoseparatetheeffect ofsizeandstrainbroadeningduetotheirdifferentdependence on the scattering angle. For the BPT and BPTC (0.1 %) samplestheX-raysynchrotronpowderdiffractiondatawere collectedatbeamlineB2synchrotronlaboratoryHASYLAB/ DESYandtheLaB6externalstandardwasusedfordetermi- nationofinstrumentalbroadeningofthediffractionmaxima. Graphical results ofWilliamson-Hallanalysis of the micro- structureofBPTandBPTCsamplesarepresentedinFig.5. Theanalysisofangulardependenceofthelinewith(HWFM) shows that the samples are characterized by similar micro- structureparameters.Theaveragegrainsizewasassessedto be of several hundred nm, and the average microstrains pa- rameters <ε> are between 0.04 and 0.05%.
Fig. 5Graphicalresults of theWilliamson-Hallanalysis of microstruc- tureoftheBPTandBPTC(0.1%)samplesbyusingsynchrotronX-raypowder diffraction data(beamlineB2atHASYLAB/DESY,λ=0.53821 Å, LaB6standard, HWFMSt=0.058–0.065deg)

(b)

JElectroceram(2014)32:92–101
97
Table 2 The enthalpyΔHobtained for BT and BPT
Substance
Temperatureofoccurrenceof peaksTc;T1; T2[K]
ΔH[J/mol]
BT
399
291
206
430
252
165
275
163
37
426
130
50
BPT
ThevaluesofΔHcalculatedforBTandBPTaresummarizedinTable2.
Figure8showstemperature variationofthe real partofthe permittivity measuredatthefrequencyof1kHz forBT,BPTand BPTCceramics.One canobserveashiftofTctowardshigher temperatures by about 30 K in the case of BPT incomparisonwith thatofBT.Theresult coincideswith thoseofour DSCstudies.TheadditionofCo3+ionsresultsin abroad-eningofthedielectric anomalyandadownwardshiftoftheCuriepoint.Inthe caseof0.1%dopingwith Co2O3the Curietemperature appearstobeshiftedby~5.5Kand thedielectricanomaly is considerably lower than that of BPT ceramics. BPTC doped with 1 % of Co2O3shows a huge dielectricanomaly shifted downwardsby~34KwithrespecttothatofBPT.Theeffect confirmstheobservationby H.JHagemannandH.Ihrig [1] forBaTiO3polycrystaldoped with Co3+.
Allinvestigated materialsdonot obey theCurie-Weisslaw aboveTC(Fig.9). ThetemperaturerangeΔTcminwhichthedeviationappearswasestimatedasthedifferenceinthetemper-atureatwhich theexperimental point divergesfromtheCurie-Weisslawandthetemperatureofminimumof1/ε′.TheaccuracyoftheΔTcmestimationweassessas±0.2K.Thisbehaviorpointstothemechanismoftheparaelectric-ferroelectrictransitioncom-posed of twocontributions:thedisplaciveand theorder—
Fig.6SEMimageofthefractureofBPTC(0.1%)ceramicsample
Figure6shows an example of the scanning electron mi- croscope(SEM)imageofafractureofBPTC(0.1%)sample. Onecanobserveindividualgrainsofaveragesizesofseveral hundred nm and theiragglomerates.
TheresultsofDSCmeasurements(Fig.7)sustainthe1st-orderdiscontinuouscharacteroftheCuriephasetransitioninBPT.At430K,one canobserveasharp peak, shiftedbyabout30KtowardshighertemperaturesincomparisonwiththatoftheBTsample.Bothstructuraltransitions:betweenthetetragonaland theorthorhombicphasesaswellasfromtheorthorhombicphasetotherhombohedraloneinBPTareloweredby~40K.InthecaseofBPTC,allphasetransitionswerefoundtobediffused.TheenthalpyΔHrelatedtoparticulartransitionsinBTandBPTcanbeevaluatedfromtheexcessspecificheatcapacity
using the following equation [30]:
T2
ðTÞ¼∫
ΔH
CpðTÞdT:
ð1Þ
T1
Fig.8Temperaturedependencesofrealpartofdielectricpermittivityε′obtained forBT,BPT,BPTC(0.1 %) and BPTC(1 %) ceramics at the frequency of 1kHz
Fig. 7 DSC curves ofBT,BPT and BPTC (0.1 %) ceramics

98
JElectroceram(2014)32:92–101
presenceofnonzero quadrupole couplingattheTisites [35,36]pointingtoacombined displaciveandorder—disordermecha-nismoftheCurietransition.Theexistenceofpolarclustersinthe paraelectricphaseinfluencesalsotheelectrostrictivepropertiesofBaTiO3becauseofthenonzerovalueofsquaredpolarizationP2
(a)
Fig.9 DeviationdegreeΔTcmfromtheCurie-Weisslawatthefrequen- cy of 100 kHz obtained forBT,BPT,BPTC(0.1 %) and BPTC(1 %) ceramics
disorderone.Inthe bariumtitanatethecentralTiionsjump betweeneightequivalent<111>off-centersitesinsidetheoxy-genoctahedra[31]. FasthoppingofTiionscoexistswith slow90° flipping of displacive soft mode induced tetragonalnanodomainsintheparaelectricphase[32].Asaconsequence,polar clusters appearand grow whenapproachingthephasetransitionfrom the hightemperature side.Alotofexperimentalmethodswasusedtoevidencebothdisplaciveandorder—disorder characterof themechanismofconductingtheCuriephasetransition.Themeasurementsoftemperaturedependenceofthebirefringence revealedtheΔnmagnitudeoftheorderof10−5up toabout30KaboveTcduetothepresenceofpolar clusters[33,34].NMRobservationofthefirstordersatellitesin47Tiand49Tispectrainthecubic phaseofBaTiO3showedthe
(b)

(c)
Fig.10Temperaturedependencesofimaginarypartofdielectricpermit- tivityε″obtainedforBT,BPT,BPTC(0.1%)andBPTC(1%)ceramicsat the frequency of 1kHz
Fig. 11 Dielectric absorption of BPT, BPTC(0.1 %) and BPTC(1 %) ceramics in the low temperature range

JElectroceram(2014)32:92–101
99
ε″bellowtheCurie transition.Themaximaarerelatedtothe contributionofdomainwallmotiontothedielectricresponse.Thecharacteristicfeaturesofthisprocessarethefollowing:1) itcanappearonlyintheferroelectric phase;2)therelaxation frequencyisstronglytemperaturedependentonlyveryclosetoTCand far below it approaches a value which is sampledependent;3)thestrengthisstronglydependentonthequalityofthematerialsointhecaseofhighdefectconcentrationitcan vanishentirely[46].Intheceramicsstudied,thedefectscanbe locatedonthedomainwallsandpintheirmotionintheexternal
Co3+
electric field [47]. After doping with
cations, i.e. for
BPTC one should notice the reduction of dielectric losses attributed to the domain wall motion in the orthorhombicphase.Theseresultsareinagoodagreementwiththatobtainedfrom themechanical results publishedin[2].WecanconfirmtheremarksbyHardtl[48] thatacceptor dopantsions fixthe domainwallposition.
Fig. 12 Arrhenius plots of electric conductivity of BPT, BPTC(0.1 %) and BPTC(1 %) ceramics measured at the frequency of 1 Hz in the temperature range 465 K–525 K
Co3+
The situation appears to be more complicated for
despitethe fact thattheremnant polarizationis notmeasurable[37].Brillouin light scattering studies[38,39]showedanoma-louschangesofacoustic phonons accompaniedbytheappear-anceofquasielasticcentralpeak onapproachingTcin theparaelectricphase.Moreover,manytheoreticalworks basedonthefirst-principle calculationsandpolarizabilitymodel[40–42]have been donetoexplainthedeviationfromCurie-Weiss be-haviorduetothecomplex dynamicsofthetransition.
The dielectric permittivity-temperature characteristic of BPTC shows the highest deviation degree from the Curie-
dopedPBTceramicsinthelow-temperature regionasshowninFig.11.Thephase transitionfrom therhombohedraltothe orthorhombicstructureapparentasε″(f,T)anomalyat~160KforBa0.95Pb0.05TiO3disappearsforcobalt doped ceramic andinthesametemperaturerangerelaxor-likerelaxationprocessesareobserved.InthecaseofBPTC(0.1%)samplesthemaxi-mumvaluesof theimaginary partofdielectricpermittivity
ε″max
decrease with increasing frequency in the window
100 Hz≤f≤6 kHz whereas at higher frequencies an increase
inε″maxisobservedandat100 kHz itsmaximum appearsatTε″max≈203 K.Accordingtothetheoryofthedielectricre-sponseofferroelectric relaxors[49,50],which considers the behaviorofε′maxandε″maxwithincreasingfrequency,i)inthe case whenε′maxdecreasesandε″maxincreaseswithincreasing frequencythe maincontributiontothedielectric responseisduetoflippingofthedipole moments between allowed direc- tionsinthepolarnanoregions(PNRs),ii)whereasadecreasein
Weiss law measured asΔTcm=Tdev−Tm[43], where
Tdev
denotesthetemperature abovewhich1/ε′startstoobeytheCurie-Weisslaw.HoweverthelowestdeviationcanbenoticedforBPT.Probably,theoriginofthiseffectishighertetragonality
(c/a=1.012)observedfor PBTbythe XRDstudy(Table1) incomparisonwiththatofBT(c/a=1.011)[44,45]andBPTC(1%)(c/a=1.010). ThedeviationsΔTcmdeterminedonthebasisofthe1/ε′dependenceontemperatureatthefrequencyof100kHzshowninFig.9are:25.9K,12.9K,41.5Kand48.9KforBT,BPT,BPTC(0.1%)andBPTC(1%),respectively.
AsseeninFig.8thedielectric anomalies associatedwithstructural transitions: fromthetetragonaltotheorthorhombicandfromtheorthorhombictotherhombohedralphasesarealso influencedbydopingofBTwithPb2+andCo3+cations.FortheBPT one canobserveashiftof theanomaliesbyabout40 Ktowardslowertemperatures.However,thedopingofBPTwithCo3+cationsresultsindiffusenessoftheanomalyrelatedtothe transitionbetweenthetetragonalandtheorthorhombicphases.Thetransitionfrom theorthorhombic phasetotherhombohe-dralone was notobservedintheinvestigated temperature and frequencyranges.
Temperaturedependencesof theimaginary partsofdielec-tricpermittivityε″showninFig.10enablefurtherexplanationoftheeffectofdopantsonthedielectric propertiesofBPTC.ForBPTonecanobservethemaximaofdielectricpermittivity
ε′max	ε″max
and
with increasing frequency is related to the
contributionoffluctuationsoftheboundariesofPNRs. Thuswewouldliketorelatethedielectric response observedinthe frequencyrange100Hz–6kHztobeduemainlytothecontri- butionoffluctuationsofPNRboundaries, whereas that appar-entinthefrequencyrange10kHz–100kHztotheresponseofthedipole momentsinthedynamic polar nanoregions. The contributionofthefluctuationsoftheboundariesofPNRsin BPTC(1%)isvisibleinthefrequencywindow100Hz–1kHz only andabove 1kHzthecontributionofdipole momentsflipping between allowed<111>cubdirectionsinPNRsdom- inatesinε″(f, T)behaviorwithTε″max≈180 K at100kHz.
Thetransitionfrom the phase with theorthorhombic struc-turetothatwiththetetragonalsymmetryappearsasanarrowε″peakat~247.5KinpureBa0.95Pb0.05TiO3ceramicswhichin
Co3+
doped ceramics becomes considerably broadened. In
BPTC(1 %) samples at frequencies higher than ~10 kHz an additional contribution to the dielectric absorption, most

100
JElectroceram(2014)32:92–101
probablyduetothedipole moments flipping between allowed
<110>cubdirections,canbedistinguished.Wedidnotdeterminetheactivation energiesEaoftheprocesses becausethemea-surements were done in a narrow frequency window (2–3frequency decades)and theresultsoffittingtoVogel-Fulcherequationwouldbeloadedwithagreaterror.
TocharacterizetheeffectofCo3+dopingonthehigh tem-perature electric properties of BPTC ceramics we show inFig.12Arrhenius plotsofelectric conductivityof theceramicsamples measuredatthefrequencyof 1 Hz inthetemperaturerange 465 K–525 K. Doping results in an increase in the conductivity by more than one order of magnitude due tooxygen vacancies introducedtocompensatetheCo3+valenceattheB-siteoftheperovskitelattice.Theactivationenergiesoftheoxygen vacancies migrationwereassessedtoamount to(0.90±0.05)eV,(0.84±0.05)eVand(0.052±0.05)eV,respec-
tivelyforBPT,BPTC(1%)andBPTC(0.1%)ceramics. The activation energyoffree oxygen vacancy migrationinferro- electric perovskite oxideshas beenreportedto be of0.8–1eV [51,52] thuswecanrelatethehigh-temperature electriccon-duction determinedfor BPT andBPTC(1%)ceramicstothe processofoxygen vacancies migration.Asthedistributionoftheoxygen vacanciesinthelatticehasbeen consideredinthe tetragonal phaseoftheferroelectric perovskitesonly[26,50,52]itishardtodiscusstheloweringoftheactivationenergyforBPTC(0.1%)sincetheenergy landscapeofoxygenandprob-ably alsoPbvacanciesisuncertain.
andtosmooththeelastic modulus anomalyinBTbasedce- ramics[2]webelievetoopenthediscussionontheeffectofa well defined polar heterogeneity at the nanoscale in oxideperovskitesontheanomaliesofphysicalpropertiesatthestruc-tural phasetransitions.
Acknowledgments The dielectric response studies weresupportedby the funds from COSTActionMP0904: Single- andmultiphaseferroics andmultiferroicswithrestrictedgeometries(SIMUFER).Thepartofthe DSCmeasurementswascarriedoutwiththeequipmentpurchasedthanks tothefinancialsupportoftheEuropeanRegionalDevelopmentFundin theframeworkofthePolishInnovationEconomyOperationalProgram(contractno.POIG.02.01.00-12-023/08).L.Vasylechkoacknowledgesa support of the Ministry of Education, Science,Youthand Sports of Ukraine(projectsDB/Neos)andtheICDDGrant-in-Aidprogram.Insitu high—temperature diffraction measurements were carried out during beamtimes allocated to HASYLAB ProjectI—20110214.
OpenAccessThis article is distributed under the terms of theCreativeCommonsAttributionLicensewhichpermitsanyuse,distribution,and reproduction in any medium, provided the original author(s) and the source arecredited.
References
1. H.J.Hagemann,H.Ihring,Valencechangeandphasestabilityof3d- dopedBaTiO3annealedinoxygenandhydrogen.Phys.Rev.B20,3871–3878(1979)
2. B.L.Cheng,M.Gabbay,W.JrDuffy,G.Fantozzi,Mechanicalloss andYoung’smodulus associated with phase transitions in bariumtitanatebasedceramics.J.Mater.Sci.31,4951–4955(1996)
3. K.Uchino,FerroelectricDevices(MarcellDekker,Inc.,NewYork-Basel, 2000), pp.105–118
4. Landolt-Börnstein,NumericalDataandFunctionalRelationshipsinScienceandTechnology,Vol.III/16a(Springer,Berlin,1981),p.421
5. Y.L.Li,L.E.Cross,L.Q.Chen,Aphenomenologicalthermodynamic potentialforBaTiO3singlecrystals.J.Appl.Phys.98,064101-1-4(2005)
6. R.F.Blunt,W.F.Love,ThedielectricpropertiesofBariumTitanateatlowtemperatures.Phys.Rev.76,1202–1204(1949)
7. G.Arlt,D.Hennings,G.deWith,Dielectricpropertiesoffine–grainedbarium titanate ceramics.J.Appl. Phys.58,1619–1625(1985)
8. H. Kishi,Y.Okino, M. Honda,Y.Iguchi, M. Imaeda,Y.Takahashi,
H. Ohsato,T.Okuda, Theeffectof MgO and rare-earth oxide on formation behavior of core-shellstructureinBaTiO3.Jpn. J. Appl.Phys.36,5954–5957 (1997)
1. J.F.Meng,B.K.Rai,R.S.Katiyar,G.T.Zou,Studyofvisibleemis- sion and phase transition innanocrystalline A(1-x)A′xTiO3systems. Phys. Lett. A 229, 254–258(1997)
2. A.V.Myasoedov,S.R.Syrtsov,Positive temperaturecoefficientof resistanceinthelead-containingceramicbariumtitanate.Tech.Phys.42,1097–1098(1997)
3. I.V.Lisnevskaya, I.A. Bobrova, E.A. Bikyashev,T.G.Lupeiko, InterfacialreactionsandpropertiesofY3Fe5O12/Ba1–xPbxTiO3com-posites.Inorg. Mater.42,1147–1151(2006)
4. J.Brančin,L.Medveck,Influenceofmechanicalactivationofpre-
cursors on the structure and properties of donor dopedBa0.95Pb0.05TiO3ceramics. J. Mater. Sci. Lett. 21, 55–59 (2002)
A.I.Lebedev,I.A. Sluchinskaya, A. Erko, A.A.Veligzhanin,A.A.Chernyshov,XAFSstudiesofthelocalenvironmentofPbimpurity atomsinbarium,strontium,andcalciumtitanates.Phys.SolidState51,991–997(2009)
4 Conclusions
Anewceramicmaterial(BPTC)wasproposedforapplicationsin the electronic industry and its dielectric properties wereinvestigated.Theexperiment confirmed thatthecontentofPb2+ionssubstitutingthe Ba2+ionsinA—siteisveryusefultooltocontroltheCurietemperature.Fromtheapplicationpointofviewit isverypromisingtheeffectofreductionofhighdielectriclosses related to thestructural phase transitioninBPTCduetodopingwithCo3+ions.Itshouldbementioned
that Pb2+and Co3+dopingofBaTiOresultsinadiffusiveness
3
andbroadeningof theferroelectric—paraelectricphasetransi-tion.Moreover,wefound that BPTCexhibits relaxor-like be- haviorinthelow-temperature range,from 125to225Kwhich speaksinfavourofthe polarnanoregions, originatingfromthe presenceofCo3+acceptor-oxygen vacancy dipolesinhighly polarizable lattice,to beresponsibleforthemodificationofthe physicalproperties.Moreover,thedielectricrelaxationprocess-esapparentintherhombohedralandtheorthorhombicphasesofCo-dopedBPTceramicsenabledtodistinguishthecontributiontothedielectric responseoffluctuationsofpolarnanoregionboundariesand thatofdipole moments reorientation betweentheallowed directionsin thepolarnanoregions.As theCo-dopinghasbeen reportedtodecreasethemechanicallosses

JElectroceram(2014)32:92–101
101
1. A.Ziębińska,D.Rytz,K.Szot,M.Górny,K.Roleder,Birefringence aboveTcin single crystals of barium titanate. J. Phys. Condens.Matter20,142202-1-5(2008)
2. M.Takagi,T.Ishidate, Anomalous birefringence of cubicBaTiO3.Solid State Commun. 113, 423–426(2000)
3. B.Zalar,V.V.Laguta,R.Blinc,NMRevidenceforthecoexistenceoforder–disorderanddisplacivecomponentsinBariumTitanate.Phys.Rev.Lett.90,037601-1-4(2003)
4. B.Zalar,A.Lebar,J.Seliger,R. Blinc, NMR study of disorder inBaTiO3andSrTiO3.Phys.Rev.B71,064107-1-12(2005)
5. K. Wieczorek, A. Ziębińska, Z. Ujma, K. Szot, M. Górny, I. Franke, J. Koperski, S. Soszyński, K.Roleder,Electrostictiveand
piezoelectriceffectinBaTiO3andPbZrO3.Ferroelectrics336,61–67(2006)
1. J.H.Ko,S.Kojima,T.Y.Koo,J.H.Jung,C.J.Won,N.J.Hur,Elastic softening and central peaks in BaTiO3single crystals above thecubic-tetragonalphase-transitiontemperature.Appl.Phys.Lett.93,102905-1-3(2008)
2. J.H. Ko,T.H.Kim, K. Roleder, D. Rytz, S. Kojima, Precursordynamicsintheferroelectricphasetransitionofbariumtitanatesingle crystals studied by Brillouin light scattering. Phys.Rev.B 84 ,094123-1-9(2011)
3. R.Migoni,H.Bilz,D.Bäuerle,Originoframanscatteringand ferro-electricityinoxidperovskites. Phys.Rev.Lett.37,1155–1158(1976)
4. I. Ponomareva, L. Bellaiche,T.Ostapchuk, J. Hlinka, J. Petzelt,Terahertzdielectric response of cubic BaTiO3. Phys.Rev.B77,012102-1-4(2008)
5. H.Bilz,G.Benedek,A.Bussmann-Holder,Theoryofferroelectric-ity:thepolarizabilitymodel.Phys.Rev.B35,4840–4849(1987)
6. J.Suchanicz,G.Stopa,K.Konieczny,D.Wcislo,M.Dziubaniuk,J.Rymarczyk,Uniaxial pressure effect on the dielectric propertiesoftheBaTiO3singlecrystals.Ferroelectrics366,3–10(2008)
7. H.D.Megaw,Crystal structure ofdoubleoxides of the perovskitetype. Proc. Phys. Soc.58,133–152(1946)
8. Y.Yoshimura,M.Morioka,A.Kojima,N.Tokunaga,T.Koganezawa,
K.Tozaki,ReinterpretationoftheunitcellevolutionofBaTiO3.Phys.Lett.A 367,394–401(2007)
1. C.Pawlaczyk, Domainwalldielectric responsein thephasetransition region in some ferroelectric. Ferroelectrics 140 , 127–132(1993)
2. K.Carl,K.H.Hardtl,Electricalafter-effectsinPb(Ti,Zr)O3ceramics.Ferroelectrics17,473–486(1978)
3. K.H. Hardtl, Electrical and mechanical losses in ferroelectric ce-ramics. Ceram. Int.8,121–127(1982)
4. A.A.Bokov,Z.-G.Ye,Low-frequencydielectricspectroscopyofthe relaxor ferroelectric Pb(Mg1/3Nb2/3)O3-PbTiO3. Phys.Rev.B65,144112-1-10(2002)
5. A.A.Bokov,Z.-G.Ye,Dielectricrelaxationinrelaxorferroelectrics.J.Adv.Diel.2,1241010-1-24(2012)
6. C.H. Park, Microscopic study on migration of oxygen vacancy inferroelectric perovskite oxide. J. Phys. Soc. 42 , S1420–S1424(2003)
7. P.Erhart,R.-A.Eichel,P.Träskelin,K.Albe,Associationofoxygen vacancieswithimpuritymetalionsinleadtitanate.Phys.Rev.B76,174116-1-12(2007)
1. Landolt-Börnstein,NumericalDataandFunctionalRelationshipinScienceandTechnology,Vol.III/28a(Springer,Berlin-Heidelberg, 1990), p. 228
2. J.H.Kim,S.H.Yoon,Y.H.Han,EffectsofY2O3additiononelectri- cal conductivity and dielectric properties of Ba-excessBaTiO3.J.Eur.Ceram. Soc.27,1113–1116(2007)
3. Y.Park,H.G.Kim,Themicrostructureanalysisofcerium–modified BariumTitanatehavingcore-shellstructuredgrains.Ceram.Int.23,329–336(1997)
4. H.Takeda,H. Harinaka,T.Shiosaki, M.A.Zubair,C. Leach, R.Freer,T.Hoshina,T.Tsurumi,Fabricationand positivetemperature coefficientofresistivitypropertiesofsemiconductingceramicsbased ontheBaTiO3–(Bi1/2K1/2)TiO3system.J.Eur.Ceram.Soc.30,555–559(2010)
5. R.A.Serway,W.Berlinger, K.A. Müller,R.W.Collins, Electron paramagnetic resonance of three manganese centers in reducedSrTi03.Phys.Rev.B16,4761–4768(1977)
6. W.Li,J.Qi,Y.Wang,L.Li,Z.Gui,DopingbehaviorsofNb2O5and Co2O3intemperaturestableBaTiO3-basedceramics.Mat.Lett.57,1–5(2002)
7. Q. Li, J. Qi,Y.Wang,Z. Gui, L. Li, Improvement of temperature- stableBaTiO3-baseddielectricsbyadditionofLi2CO3andCo2O3.J.Eur.Ceram. Soc.21,2217–2220(2001)
8. S.Zhang,J.B.Lim,H.J.Lee,T.R.Shrout,Characterizationofhard piezoelectriclead-freeceramics.IEEETrans.Ultrason.Ferroelectr.Freq. Control56,1523–1527(2009)
9. L.E.Cross,Relaxorferroelectrics:anoverview.Ferroelectrics151,305–320(1994)
10. A.A.Bokov,Z.-G.Ye,Recentprogressinrelaxorferroelectricswith perovskite structure. J.Mater.Sci.41,31–52(2006)
11. G.A.Samara,Therelaxational propertiesofcompositionally disorderedABO3perovskites.J.Phys. Condens. Matter15,R367–R411(2003)
12. M.E. Lines, A.M. Glass,Principle and application offerroelectricandrelatedmaterials(Clarendon, Oxford,1977)
13. G.Arlt,H.Neumann,Internalbiasinferroelectricceramics:origin and time dependence. Ferroelectrics87,109–120(1988)
14. R.Bujakiewicz-Korońska,A.Kalvane,Y.Zhydachevskii,B.Garbarz- Glos,W.Śmiga,L.Vasylechko,J.Czerwiec,A.Suchocki,A.Kamińska,
W.Piekarczyk, Physical PropertiesofBa0.95Pb0.05TiO3+0.1%Co2O3.Ferroelectrics436,62–71(2012)
1. M.C. Baehtz, H. Ehrenberg, H. Fuess, The synchrotron powderdiffractometerat beamline B2 atHASYLAB/DESY:status and ca- pabilities. J. Synchrotron Radiat. 11, 328–334(2004)
2. L.G.Akselrud,P.Y.Zavalij,Y.Grin,V.K.Pecharsky,B.Baumgartner,E.Wölfel,Use of the CSD programme package for structuredeterminationfrompowderdata.Mater.Sci.Forum133,335–340(1993)
3. G.W.H.Höhne,W.F.Hemminger,H.-J.Flammersheim,DifferentialScanningCalorimetry(Springer,BerlinHeidelberg,2003),p.140
4. R.Pirc,R.Blinc,Off-centerTimodelofbariumtitanate.Phys.Rev.B
70, 134107-1-8 (2004)
A.Bussmann-Holder,H.Beige,G.Völkel,Precursoreffects,broken localsymmetry,and coexistence oforder–disorderand displacive dynamicsinperovskiteferroelectrics.Phys.Rev.B79,184111-1-6(2009)