# NOEA 2011
International Symposium
on
Nitrogen Oxides Emission Abatement
Book of Abstracts
Edited by
J.	BARTYZEL, P. KORNELAK, M. NAJBAR
4-7 September 2011
ZAKOPANE, Poland
Symposium finansed by WND-POIG. 01. 01. 02-12-112/09
co-financed by the European Regional Development Fund
under the Innovative Economy Operational Programme 2007-2013

ISBN 978-83-233-3249-7
Wydawnictwo Uniwersytetu Jagiellońskiego
Redakcja: ul. Michałowskiego 9/2, 31-126 Kraków tel. 12-631-18-81, 12-631-18-82, fax 12-631-18-83 Dystrybucja: tel. 12-631-01-97, tel. /fax 12-631-01-98 tel. kom. 506-006-674, e-mail: sprzedaz@wuj. pl

##### CONTENTS
PREFACE	9
Maria Skłodowska-Curic - a heritage of the 19th and the legacy to the 21 st century
PETELENZ	11
Maria Sktodowska-Curie in philately, numismatics and medallic art
J. BARTKE	13
Maria Sktodowska-Curie as a role model for scientists
A. RAFALSKA-ŁASOCHA	15
Treatment of off-gases containing NOX by electron beam
A. G. CHMIELEWSKI, J. LICKI, A. PAWELEC, Z. ZIMEK, Y. SUN, S. WITMAN	17
Plasma assisled-deNOx catalysis
G. DJEGA-MARIADASSOU	19
Performance of the plasma treatment catalyst compared with a classical thermal on alumina catalysts: an approach to NOX abatement
M. FOIX, C. GUYON, M. TATOULIAN, P. Da COSTA	21
State-of-the-art nitrogen oxide removal from off-gases of stationary sources by ammonia
M. A. BUZANOWSKI	23
Simultaneous NO reduction and soot oxidation on transition metal oxide catalysts
M. NAJBAR, E. PAŁKOWSKA, J. DUTKIEWICZ,
NAZARCZUK, L. LITYŃSKA-DOBRZYŃSKA, E. BIELAŃSKA,
WESEŁUCHA-BIRCZYŃSKA. W. IASOCHA, J. CAMRA, M. KOZICKI	25
Modelling of structured reactor based on wire gauzes and zeolite catalyst for ammonia reduction of NOX from biogas turbines
P. JODŁOWSKI, J. OCHOŃSKA, D. Mc CLYMONT,
GIL, A. KOŁODZIEJ, S. KOŁACZKOWSKI, J. ŁOJEWSKA	27
Copper exchanged zeolite in structured reactor based on wire gauzes for ammonia reduction
of nitrogen oxides from biogas turbines
J.	OCHOŃSKA, A. KNAPIK, D. Me CLYMONT,
A. ROGULSKA, P. JODŁOWSKI, B. GIL W MAKOWSKI,
A. KOŁODZIEJ, S. KOŁACZKOWSKI, J. ŁOJEWSKA	29
NOx removal from stationary sources by selective catalytic reduction
A. E. PALOMARES	31
Modified clay minerals as effective catalysts of the DeNOx process
L. CHMIELARZ	33
Modified carbonaceous materials in DeNOx reaction
T. GRZYBEK, J. KLINIK, M. MOTAK, B. SAMOJEDEN	37
HC SCR as alternative process for NOX abatement in stationary and mobile sources
P. Da COSTA	41
3

Effect of Cl and C2 organic reducing agents on selective catalytic reduction of NO on FeSiBEA and CoSiBEA zeolites
J. JANAS, W ROJEK, S. DŹWIGAJ	43
DeNOx assisted by hydrocarbons
AISSAT, D. COURCOT, S. SIFFERT	45
Influence of the crystallite size of nobel metals on the course of the DENOX reaction
D. NAZIMEK, W ĆWIKŁA-BUNDYRA	47
Structural-functional design of catalysts for gas emissions purification from nitrogen (I), (II) oxides
S. ORLYK, S. SOLOVIEV, T. BOICHUK, P. KIRIENKO	49
Strategy of NOX reduction for the Diesel engines of light passenger cars
J. -M. TRICHARD	53
Selective Catalytic Reduction of NOX by diesel fuel: plasma-assisted HC/SCR system
K. CHO, J. -H. LEE, C. C. CRELLIN, K. OLSON,
D. L HILDEN, M. K. KIM, P. S. KIM, I. HEO, I. -S. NAM	55
Catalytic behavior of combined LNT/SCR systems
P. FORZATTI, L. LlETTl, L CASTOLDI, R. BONZI,
S. MORANDI, G. GHIOTTI, S. DŹWIGAJ	59
Effect of thermal aging on surface morphology and performances of commercial Lean NOX Traps
ADOUANE, P. Da COSTA, P. DARCY	61
Modelling of N2O formation during the regeneration of NOX storage catalyst
Ś. BARTOVA, P. KOCI, M. MAREK, J. PIHL, J. -S. CHOI, W PARTRIDGE	63
NO reduction by H2 on Rh-based catalyst for Natural Gas vehicles:
Study of active sites by operando IR spectroscopy
S. CARRE, Y. RENEME, F. DHAINAUT, C. DUJARDIN, P. GRANGER	67
Controlling the surface dispersion of bao nano-domains on catalytic NOX storage materials
via TiO2 anchoring sites and improvement of sulfur poisoning tolerance
ÓZENSOY, G. SEDA $ENTURK, E. VOVK	69
NOx reduction and methane oxidation over mesoporous silica supported palladium
J. BASSIL, A. AIBARAZ1, P. Da COSTA, M. BOUTROS	71
Design of the Catalysts for the Removal of Diesel Soot and NOX
Z. ZHAO	75
Catalytic filters for the simultaneous removal of soot and NOX:
influence of the alumina precursor on monolith washcoating and catalytic activity
M. E. GALVEZ, S. ASCASO, 1. TOBIAS, R. MOLINER, M. J. LAZARO	77
Silver-based catalysts for NOX SCR with ethanol: a mechanistic study on Ag/ZSM-5 and Ag/AI2O3
A. WESTERMANN, R. BARTOLOMEU, B. AZAMBRE, R. BERTOLO,
HENRIQUES, A. KOCH, P. Da COSTA, M. F. RIBEIRO	81
4

Investigation of Cs-Cu/ZrO2 systems for simultaneous NOX reduction
and carbonaceous particles oxidation
A. AISSAT, D. COURCOT, S. SIFFERT	83
Effect of water on NO decomposition over Cu-ZSM5 based catalysts
G. LANDI, L LISI, R. P1RONE, G. RUSSO, M. TORTORELLI	87
Hysteresis effect study on Diesel Oxidation Catalyst for a better efficiency of SCR systems
A. MANIGRASSO, N. FOUCHAL, P. DARCY, P. Da COSTA	89
lx>w temperature N2O decomposition over nano oxide catalysts
A. KOTARBA, G. MANIAK, P. STELMACHOWSKI, W PISKORZ, F. ZASADA, Z. SOJKA	91
The influence of structural promolors on the activity of iron oxide based catalyst for N2O decomposition
P. KOWALIK, K. STOLECKI, K. MICHALSKA, J. KRUK, M. KONKOL	93
Stoichiometric and non-sloichiometric Perovskite-based catalysts
for the catalytic decomposition of N2O from nitric acid plants
Y. WU, X. NI, P. GRANGER, C. DUJARDIN	95
N2O catalytic decomposition - from laboratory experiment to industry reaktor
L. OBALOVA, K. JIRATOVA, F. KOMANDA	97
The application of metallic iron for N2O reduction al higher temperature and oxygen presence
J. LASEK, B. GRADOŃ	99
Copper ionic pairs as active sites in N2O decomposition on CuOx/CeO2 catalysts
A. ADAMSKI, W. ZAJĄC, F. ZASADA, Z. SOJKA	101
Dual role of surface nitrate species formed during NOX activation on supported oxometallic TM1 clusters
4. ADAMSKI, M. FIUK, M. TARACH, P. ZAPAŁA, B. GIL, Z. SOJKA	107
Comparison between Cs-Cu/ZrO2 and Cs-Co/Zr02 catalysts for NOX reduction in the presence of toluene
AISSAT, D. COURCOT, S. SIFFERT	111
On the influence of exhaust gas composition for the selective reduction of NOX over Fe/ZSM-5 catalyst
ADOUANE, J. STARCK, P. Da COSTA, X. JEANDEL	115
DRIFTS-MS studies of NO reduction and NH3 oxidation over V-O-V catalyst
AZAMBRE, J. BANAŚ, M. NAJBAR	117
SEM -EDS studies of transition metal catalysts for NO decomposition
BIELAŃSKA, M. ZIMOWSKA, I. NAZARCZUK, M. KOZICKI, M. NAJBAR	119
XPS studies of Ni-Cr-Fe oxide catalysts for NO decomposition
J. CAMRA, J. DUTKIEWICZ M. KOZICKI, M. NAJBAR	121
Acid-activated vermiculites as catalysts of the DeNOx process
CHMIELARZ, M. WOJCIECHOWSKA, M. RUTKOWSKA,
A. WĘGRZYN, A. ADAMSKI, B. DUDEK, R. DZIEMBAJ,
A. MATUSIEWICZ, M. MICHALIK	123
Is Hydrogen the main NOX reducing agent at low temperature for a CNG 3-way catalysts?
M.	ADAMOWSKA, S. CAPELA, M. SALAUN, L. GAGNEPAIN, P. Da COSTA	127
5

Influence of the ion exchanged metal (Cu, Co, Ni and Mn) on the selective catalytic reduction of NO over mordenite and ferierite
W. ĆWIKŁA-BUNDYRA	131
Structural studies and physicochemical properties of new molybdenum peroxocomplexes with nicotinic acid
A. DOBIJA, W. NITEK, W ŁASOCHA	135
Effect of soot on NO decomposition in O2 and SO2 presence over Ni-Cr-Fe oxide catalysts
J.	DUTKIEWICZ, S. JAN1GA, I. NAZARCZUK, M. KOZICKI, P. KORNELAK, M. NAJBAR	137
Surface, structural and morphological characterization of nanocrystalline ceria-zirconia mixed oxides upon thermal aging
/. DOBROSZ-GÓMEZ, M. A. GÓMEZ-GARCIA, M. 1. SZYNKOWSKA,
I. KOCEMBA, J. M. RYNKOWSKI	139
Nanostructured Co-Ce-0 systems for catalytic decomposition of N2O
R. DZIEMBAJ, M. M. ZA1TZ, M. RUTKOWSKA, M. MOLENDA, L CHMIELARZ	141
Membrane reactor for ammonia decomposition - design guides
M. A. GÓMEZ-GARCIA, I. DOBROSZ-GÓMEZ, J. FONTALVO, J. M. RYNKOWSKI	143
IR studies of the coadsorption of CO and electron donor molecules on Cu+ sites in CuZSM-5 zeolite
K.	GÓRA-MAREK	147
The simultaneous SCR of N2O and NOX on Co-Na-MOR using CH4 alone as the reducing agent
M. C. CAMPA, V. INDOVINA, D. PIETROGIACOMI	149
In situ FT-IR spectroscopic investigation of gold supported on lungstated zirconia as DeNOx catalyst
M. KANTCHEVA, M. MILANOVA	151
Co-Mn-Al mixed oxide supported on TiO2 for N2O decomposition
K.	KARASKOVA, Ż. CHROMCAKOVA, S. STUDENTOVA, L. OBALOVA, K. JIRATOVA	155
Photocatalytic decomposition of N2O on Ag-TiO2
K.	KOCI', S. KREjdKOVA, Z. ŁACNY, O. SOLCOVA, L OBALOVA	159
Effect of V concentration in niobium-rich V-O-Nb/anatase catalysts
on their activity in ammonia assisted DENOX
P. KORNELAK, A. BIAŁAS, D. RASIŃSKA, J. CAMRA, W ŁASOCHA,
W ZHANG, D. SU, A. WESEŁUCHA-BIRCZYŃSKA, M. NAJBAR	163
Alloying effect on NO direct decomposition over high surface area Rh/AI2O3 catalysts
A. PIETRASZEK, P. Da COSTA, P. KORNELAK, B. AZAMBRE, L. ZENBOURY, M. NAJBAR	165
NO decomposition over Mo-V oxide bronzes
P. KORNELAK, M. ŁABANOWSKA, W MACYK, M. TOBĄ, I. NAZARCZUK, M. NAJBAR	167
Effect of surface potassium doping and NOX addition on catalytic activity
of iron and cobalt spinels in soot combustion
P. LEGUTKO, P. STELMACHOWSKI, A. KOTARBA, Z. SOJKA	169
TEM studies of transition metal oxide catalysts for NO decomposition
LITYŃSKA-DOBRZYŃSKA, K. STAN, M. KOZICKI, M. NAJBAR	171
6

DRIFT study of dcNOx reaction over Cu/CeZrO2 catalyst A. ŁAMACZ, 4. KRZTOŃ, G. DJEGA-MARIADASSOU	173
XRD study of oxide Ni-Fe-Cr catalysts for NO decomposition W. ŁASOCHA, A. RAFALSKA-ŁASOCHA, I. NAZARCZUK, M. NAJBAR	175
Modified Synthetic Spinels as Catalysts for Low Temperature deN2O
G. MANIAK, F. ZASADA, W PISKORZ, P. STELMACHOWSKI, A KOTARBA, Z. SOJKA	177
The use of DESONOX type catalysts to remove nitrogen oxides during coal combustion A. MARCEWICZ-KUBA	179
Multi-step TPSR/QMS technique to study kinetics of NO, SR with ammonia
D. Mc CLYMONT,, J. OCHOŃSKA, S. KOŁACZKOWSKI, J. ŁOTEWSKA	181
N2O formation during lean NOX reduction by hydrocarbons over a conventional DOC
MRAĆEK, S. BARTOVA, F. PLAT, P. KOCI, M. MAREK	183
Effect of O2, SO2 and H2O on NO decomposition over Ni-Cr-Fe oxide catalysts
J. DUTKIEWICZ, S. JANIGA, I. NAZARCZUK, M. KOZICKI, P. KORNELAK, M. NAJBAR	187
NOX uptake and storage properties of BaOx/Pt( 111) model catalyst:
influence of Ba coverage, surface morphology and stoichiometry
OZENSOY, E. VOVK, E. EMMEZ	189
Selective Catalytic Reduction of NOX by C2H5OH over Ag/Al2O3/cordierite
N. POPOVYCH, P. KIRIENKO, S. SOLOVIEV	191
Study of the interaction of NOX and NH3 with the surface of copper
and nickel catalysts supported on ceria-zirconia by FT-IR spectroscopy
M.	RADLIK, A. ŁAMACZ, A. KRZTOŃ, W. TUREK	193
Catalytic reduction of NO by CO over FexSiBEA catalysts I. HNAT, I. KOCEMBA, J. RYNKOWSKI, S. DŹWIGAJ	195
Preparation and characterization ofTiO2 based plasma sprayed catalytic coatings for NOX abatement V SNAPKAUSKIENE, V. VALINCIUS	197
MgF2-MgO system as a potential support for NiO catalysts for NOX reduction by propene M. ZIELIŃSKI, I. TOMSKA-FORALEWSKA, M. PIETROWSKI, M. WOJCIECHOWSKA	201
Raman spectroscopic studies of the oxide Ni-Fe-Cr catalysts for NO decomposition
A. WESEŁUCHA-BIRCZYŃSKA, M. KOZICKI, M. NAJBAR	205
Metal-supported sulfated ceria-zirconia catalysts for the SCR of NOX by ethanol: performances and mechanisms
A. WESTERMANN, B. AZAMBRE, A. KOCH	207
INDEX	211
7

PREFACE
Interest in nitrogen oxides emission abatement has been steadily growing for years both in academic and industrial research. NOEA 2011 lies also in this field. The symposium is a continuation of the annual seminars organized by Jagiellonian Universityand Marie Curie-Sklodowska University since 1994 and followed by International Symposiaon Air Pollution Abatement (2003), Air Pollution Abatement Catalysis (2005) and Air and Water Pollution Abatement (2007).
This year the organizer - Faculty of Chemistry of Jagiellonian University - invitedthe research community to discuss the following topics, at the both global and molecular level:
- NO removal from off-gases of stationary sources of emission,
- NO reduction in exhaust gases of mobile sources of emission,
- Simultaneous NO reduction and particles' oxidation,
- N2O removal.
A small introductory session is devoted to hundred anniversary of Maria Sklodowska-Curie Nobel Prize in the field of chemistry.
38 oral (6 plenary lectures, 14 keynote lectures and 18 communications) as well as 39 poster presentations covering all these subjects form the mainstream of the symposium.
Internationally renowned researchers were invited to give overview of various important areas:
- Dr. Mark A. Buzanowski, On the state-of-the-art of NO removal from off-gases of stationary sources by ammonia,
- Prof. Lucjan Chmielarz, Modified clay minerals as effective catalysts of the DeNOx process,
- Prof. Andrzej G. Chmielewski, Treatment of off-gases containing NOx by electron beam,
- Prof. Patrick Da Costa, HC SCR as alternative process for NOx abatement in stationary nd mobile sources,
- Prof. Gerald Djega-Mariadassou, Plasma assisted-deNOx catalysis,
- DSc Stanislaw Dźwigaj, Effect of C| and C2 organic reducing agents on selective catalytic reduction of NO on FeSiBEA and CoSiBEA zeolites,
- Prof. Pio Forzatti, Catalytic behavior of combined LNT/SCR systems,
- Prof. Teresa Grzybek, Modified carbonaceous materials in DeNOx reaction,
- Prof. Andrzej Kotarba, Low temperature N2O decomposition over Nano Oxide Catalysts,
- Prof. Dobiesław Nazimek, Influence of the crystallite size of nobel metals on the course of the DENOX reaction,
- Prof. Lucie Obalova, N2O catalytic decomposition - from laboratory experiment to industry reactor,
- Prof. Svitlana Orlyk, Structural-functional design of catalysts for gas emissions purification from nitrogen(l), (II) oxides,
- Prof. Antonio Eduardo Palomares, NOX removal from stationary sources by selective catalytic reduction,
- Prof. Stephane Siffert, DeNOx assisted by hydrocarbons,
- Prof. Jean-Michel Trichard, NOx emission reduction: Passenger car manufacturer point of view,
- Prof. Zhen Zhao, Design of catalysts for emissions abatement of diesel soot and NOx,
The organisers hope that this symposium will promote further discussion on the important issues of environmental protection and lead to closer cooperation of researchers interested in this field.
The NOEA Symposium is organised in framework of the POIG project "Innovative catalysts for direct NO decomposition on the base of oxide bronzes
Organising Committee
9

NOEA2011
Zakopane 4-7 September 2011
POI
##### Maria Skłodowska-Curie - a heritage of the 19th and the legacy to the 21st century
##### B. PETELENZ1
1 The Henryk Niewodniczański institute of Nuclear Physics, Polish Academy of Sciences,
152 Radzikowskiego St., 31-342 Kraków, Poland,
e-mail: barbara.petelenz@ifj.edu.pl
The year 2011 has been proclaimed by the IUPAC and UNESCO as the International Year of Chemistry. This coincides with the centenary of the Nobel Prize in Chemistry 1911, awarded to ‘Marie Curie, nće Skłodowska, in recognition of the discovery of polonium and radium, isolation of radium, and further studies on this remarkable element’. So far, Marie Curie has been the only woman awarded with two Nobel Prizes. In 1903, Marie and Pierre Curie shared the Nobel Prize in Physics with Antoine Henri Becquerel, the discoverer of radioactivity.
The pioneering studies on radioactivity were the subject of the Marie Curie’s doctorate research. Their consequences went far beyond the extension of the periodic table by two new elements. A chain of discoveries, made by Marie Curie and her contemporary scientists, revolutionized the existing views on the structure of Matter and initiated the development of modem physics and chemistry, as well as nuclear technologies.
The intellectual and emotional heritage of Maria Skłodowska-Curie was the 19th century positivism which, generally, means a philosophy of sciences, and in partitioned Poland it meant also a political program of national resistance, focused on creating a material infrastructure and educating the public. Both senses were conspicuous in Maria’s research methods, in her teaching, in the organization of the Radium Institutes, and in her war effort. She truly believed in the positivist idea that the Science should serve the Humanity.
Radium started to serve the Humanity promptly. Discovered in 1898, it was first used for radiation therapy in 1901. Very shortly, Pierre and Marie Curie realized that benefits from its applications are dramatically entangled with threats. Aware of this duality, Marie Curie always taught that applied science must be based firmly on the fundamental research. In the 21s1 century, it is worth remembering too.
11

NOEA 2011
Zakopane 4-7 September 2011
KOI
##### Maria Skłodowska-Curie in philately, numismatics and medallic art
##### J. BARTKE1
The Henryk Niewodniczański Institute of Nuclear Physics, Polish Academy of Sciences
152 Radzikowskiego St., 31-342 Kraków, Poland
Philately and numismatics is not just stamp or coin collecting: numismatics is an auxilliary branch of human history, and philately is on its way towards a similar status. Also, stamps and coins, items which are issued in large quantities, offer wide publicity and promotion for a person or an event, and it is this aspect that will be explored in this presentation.
Maria Skłodowska-Curie (MSC) has been featured on about one hundred postage stamps from many countries (on half of them she appears together with her husband Pierre Curie), and also on other philatelic items such as postal stationery or special cancellations. We will show some more interesting specimens, with emphasis on the ones presenting the “chemical aspects” of her activity, related to her discoveries of the new chemical elements polonium and radium, and to her Nobel Prize in chemistry awarded in 1911.
The earliest stamp featuring MSC was issued in Turkey in 1935 on the occasion of the International Women's Congress in Istanbul. Some issues from years 1938-1949 carried an extra charge for the anticancer campaign. Many stamps were issued at various MSC anniversaries, but she appeared also in the category of “Nobel Prize winners” or simply among “famous people”.
The effigy of MSC can also be found on Polish and French banknotes and coins, which will be presented as well.
Medallic art is of a somewhat different character. Commemorative medals, usually created in a limited number by renowned artists, are small pieces of art, paying tribute to a famous person or to a remarkable event The first medal featuring MSC was issued in Poland as early as 1934 (shortly after her death), and the first French medal in 1938 to commemorate the 40lh anniversary of the discovery of radium. The medal created in the USA in 1966 for Poland's Millenium features MSC together with Mieszko I, the founder of the Polish state, and Nicolaus Copernicus, as the three most important personalities in one thousand years of Polish history. An interesting Czechoslovak medal of 1967 evokes Jachymov Valley (St. Joachimsthal) as the place from which the uranium ore for the Curies came.
13

NOEA2011
Zakopane 4-7 September 2011
K02
##### Maria Skłodowska-Curie as a role model for scientists
##### A. RAFALSKA-ŁASOCHA1
1 Faculty of Chemistry, Jagiellonian University, 3 Ingardena St., 30-060 Krakow, Poland,
e-mail: rafalska @ chemia, uj. edu.pl
Maria Skłodowska (1867-1934) spent her youth in Poland, but during and after studies she lived and worked in France. Coincidence of many circumstances caused that she had two fatherlands. Her discoveries to the benefit of the mankind, however, made her a national of the whole world.
In 1893, Maria Skłodowska obtained the bachelor degree in physics at Sorbonne with the first honour position and in 1894 the bachelor degree in mathematics with second honour position. Then she relumed to Poland to search for a suitable job. Very soon she realized that there was not a suitable position for her. Prof. August Witkowski, who was always willing to help her, was not even able to offer her the assistant position at his Chair of Physics at the Jagiellonian University in Krakow. In Poland which was in those times divided between three invaders: Austria, Russia and Prussia, she would have had to be excluded from the academic life without which she would not have had the opportunity to apply her knowledge and skills and satisfy her justified ambitions. This is why she decided to come back to France where in 1895 she married Pierre Curie and worked with him in his lab.
After discovery of new chemical elements Maria and Pierre worked in a very hard conditions but were always cautious about the privatization of research. At the beginning of the career, they deliberately did not patent their technique for purifying radium so others would be able to conduct research on it more easily. When later, thanks to women of America, Maria received the gram of radium for research, she insisted on giving control of the radium to the University of Paris upon her death. Her co-workers retained full access for research purposes but the radium itself passed into the public’s hands.
As a scientist and a human being Maria Skłodowska Curie was and still is a worldwide hero. She was invited for the Solvay Conferences, conferred honoris causa doctorates by many universities and apart from two Nobel Prizes she was awarded many other scientific honors. However, for this modest personality, the matters of science were the most important. When she was asked to write a few words on the occasion of the tenth anniversary of regaining independence by Poland, she wrote words which are regarded as her scientific testament:
-To develop scientific laboratories which Pasteur called „sacred shrines of mankind",
■to take care of those who work for science craving knowledge in order to attain workers for the future,
-to create conditions for the innate talents and precious gifts might be realized and serve for the idea means lead the society through the way of development of power both spiritual and material.
These and other values represented by Maria Sklodowska-Curie are still up-to date for the people all over the world. Not only for Poles is she a symbol of personality of the highest moral value and highest scientific qualifications. After her death, Albert Einstein in the telegram of sympathy to her family expressed it as follows:
“Now, when the life of such an outstanding personality as Mrs Curie was ended we mustn't only limit our memories about her to that what the fruits of her work have given the humanity. The moral values of the exceptional personality have perhaps a deeper meaning for the given generation and for the whole course of the history then the intellectual achievements only. “
15

NOEA2011
Zakopane 4-7 September 2011
P02
##### Treatment of off-gases containing NOX by electron beam
##### A. G. CHMIELEWSKI13, J. LICKI2, A. PAWELEC*, Z. ZIMEK1, Y. SUN1, S. WITMAN1
1. Institute of Nuclear Chemistry and Technology, Warsaw, Poland
2. Institute of Atomic Energy, Świerk, Poland
3. Warsaw University of Technology, Department of chemical and Process Engineering,
   Warsaw, Poland
Electron beam flue gas treatment is well developed flue gas treatment technology for simultaneous SOx and NOx removal and generating usable product - fertilizer being a mixture of ammonium sulfate and nitrate. The biggest industrial plant has been built in EPS Pomorzany, Szczecin where it treats 270 000 Nm3/h and a power of accelerator installed exceed 1 MW. These one of the cold plasma technologies successfully applied in industry. Beside the gas purification for coal fired boilers, the process is well suitable for high sulfur oil fired boilers as well. The recent studies have illustrated possibility of this technology application for volatile, non methane, organic pollutants and mercury treatment. The main consumption of the energy is devoted to the NOx removal, high efficiency SOx removal is achieved at low energy deposition dose. Therefore different methods for energy consumption reduction are searched for. One of the method is applying of the gas flow patterns at double gas irradiation dose, which ensure good distribution of energy distribution field. Other method is applying a special scavengers to enhance radical driven reactions in the gaseous phase. The developments of the technology and reducing of the energy consumption may lead to the most difficult applications as a huge Diesel engine exhaust gases treatment, which the problem is not solved up to now.
The plasma processes including electron beam generated plasmas are being developed in the frame of BalticNet - PlasTEP project towards the broader technology applications.
17

NOEA2011
Zakopane 4-7 September 2011
K03
#### Plasma assisted-deNOx catalysis
#### G. D.IEGA-MARIADASSOU12
Universite Pierre et Marie Curie, UPMC Paris 6, Laboratoire Reactivite de Surface, UMR CNRS 7609, 4 place Jussieu, Case 178 Tour 54-55, 75252 Paris Cedex 05, France 2 Centrum Materiałów Polimerowych i Węglowych PAN, 41-800 Zabrze, ul. Curie- Sklodowskiej 34, Poland
Role of non-thermal plasma
Starting from a review of literature, - more particularly from the numerous papers already published
by the Society of Automotive Engineers (SAE) and comparing to chemistry of non-thermal plasma and
to molecular models of deN()x process, the present key-note will demonstrate that a non-thermal plasma
can substitute two functions (NO to NO2, and NO2 mild HC oxidation to CxHyOz oxygenates) of the
general three-lunction deNOx catalysis over supported metal cations (Mn+). The main feature is that
efficient catalysts are only working in a given range of temperature where the three functions turn over
simultaneously, whereas non-thermal plasma is working (2 functions) in the full range of temperature 11-4]
(Fig. I).
Figure I. Comparison of Catalysts activity and that of non-thermal plasma vs. Temperature
The preceding model can help to understand how the plasma assisted-deNOx catalysis is working [1-4].
The three-function model of deNO„
Three-way and dcN()x catalysis follow the same general catalytic sequence [5-8]: NO decomposes on the active site (Mn+), leading to N2 and O(ads), and the reaction is then controlled by the oxygen scavenging process through a reaction between the adsorbed reductant and O(ads). Depending on the catalytic process (TWC or deNOx), the nature of the active site varies (M° and Mn+), as well as the reductant.
19

NOEA201I
Zakopane 4-7 September 2011
In both M° and Mn+ cases, the system needs a reductant to “regenerate” the active site: CO in the case of a stoichiometric mixture (TWC), and an activated hydrocarbon (HC —> CxHyOz) or the initial HC in lean conditions (deNOx). In all cases, NO dissociation or “global reduction” to N2 (Function 3 in dcNOx model over metal cations) goes through:
- the adsorption of, at least, two NO molecules;
- the dissociation of 2NO leaving 2O(ads);
- the necessity, for a reductant, to scavenge the 2O(ads), for recovering the free sites and permitting the catalytic cycle to tum over.
The very important and interesting point in both TWC and deNOx processes is the simultaneous activation of NO(ads) and reduclant(ads) as evidenced by transient temperature programmed reactions, leading to the ‘assisted’ reduction of NO by this reductant (Fig. I).
There is never a direct interaction between NO and the reductant, but rather two main steps: decomposition of NO and oxygen-scavenging by the reductant.
Main objectives
The aim of the key-note concerns:
1. the state of the art of the non-thermal plasma/catalyst coupling, summarizing the global main results (activation of hydrocarbons, speciation of stable species at the outlet of the plasma reactor, active catalytic materials...),
2. the short presentation of the three-function model of deNOx,
3. the speciation of stabilized molecules produced during the plasma/gas phase interaction. A typical gas mixture will be: decane - toluene - propene - propane - NO - H2O - O2 - Ar mixture.
Non-Thermal Plasma Assisted Catalytic NOX Remediation from a lean Model Exhaust will be studied: experimental device; on-line analysis of reaction products, effect of energy deposition, concept of composite catalyst, reaction in the presence of exhaust gases.
1. O. Gorce, H. Jurado, C. Thomas, G. Djega-Mariadassou, A. Khacef, J-M. Cormier, J-M. Pouvesle, G. Blanchard, S. Calvo, Y. Lendresse, “Non-Thermal Plasma Assisted Catalytic NOx Remediation from a Lean Model Exhaust”, (2001) SAE Technical Paper series, 2001-01-3508, Non-thermal plasma emission control systems (SP-1639), SAE IntemationakThe Engineering Society for Advancing Mobility Land, Sea, Air Space (2001)
2. F. Baudin, P. Da Costa, C. Thomas, S. Calvo, Y. Lendresse, S. Schneider, F. Delacroix, G. Plassat, G. Djega-Mariadassou, “NOx reduction over CeO2-ZrO2 supported iridium catalyst in the presence of propanol”, (2004) Topics in Catal., 30-31, pp. 97-102
3. G. Djega-Mariadassou, M. Berger, O. Gorce, J. W. Park, H. Pemot, C. Potvin, C. Thomas, P. Da Costa, “Chapter 5. A three-function model reaction for designing deNOx catalysts”, (2007) Studies in Surface Science and Catalysis, 171, pp. 145-173
4. G. Djega-Mariadassou, F. Baudin, A. Khacef, P. Da Costa, “Chapter 4. NOx abatement by plasma­catalysis”, (2010) In: “Plasma-catalytic processes: Activation of molecules and environmental applications”, VasileParvulescu and Dr. Monica Magureanu Eds., John Wiley & Sons Ltd, submitted for publication
5. G. Djega-Mariadassou, Catal. Today 90 (2004). 27
6. G. Djega-Mariadassou, M. Boudart, J. of Catal., 216 (2003). 89
7. G. Djega-Mariadassou, F. Fajardie, J.-F. Tempere, J.-M. Manoli, O. Touret, G. Blanchard, J. of Mol. Catal. A: Chemical 161 (2000). 179
8. M. Boudart, G. Djega-Mariadassou, in Cinetique des Reactions enCatalyse Heterogene, Masson, Paris, 1982, M. Boudart, G. Djega-Mariadassou, in “Kinetics of Heterogeneous Catalytic Reactions”, Princeton, University Press, Princeton, NJ, 1984
20

NOEA2011
Zakopane 4-7 September 2011
CO I
##### Performance of the plasma treatment catalyst compared with a classical thermal on alumina catalysts: an approach to NOX abatement
##### M. FOIXU, C. GUYON2, M. TATOULIAN2, P. Da COSTA**
1. Universite Pierre et Marie Curie, Paris 6, Laboratoire de Reactivite de Surface - CNRS UMR
   7197, 4 Place Jussieu, 75252 Paris 05, France, e-mail: marjorie.foix@etu.upmc.fr
2. Ecole Nationale Superieure de Chimie Paris - Chimie ParisTech, Laboratoire “Genie des
   Procedes Plasmas et Traitement de Surface”, 11 rue P. et M. Curie, 75231 Paris cedex 03,
   e-mail: cedric.guyon@enscp.fr
*Dr. P. Da Costa, tel: + 33 1 44 27 55 12, e-mail: patrick.da_costa@upmc.fr
Catalysis is the enabling technology in a large number of processes for the provision of clean energy, and for pollution abatement. Heterogeneous catalysis occurs at the interface between a gas or liquid and a solid catalytic surface; the surface of a catalytically active solid provides an energy landscape which enhances reactivity. The use of plasma systems in catalysis is now well established (Brockhaus and al. [ I ], Xia and al. [2J, Karches and al. [3, 4]). Plasma treatments, in low pressure systems, have been already studied, in order to try to replace the thermal calcinations of catalysts. On the other hand, fluidized bed reactors offer the possibility to perform homogenous pre-treatments and have the additional advantage of excellent heat transfer rales between the gas and catalysts particles (Jafari and al. [5]) Thus, the combination of a plasma pre-treatment, carried out in a fluidized bed reactor, is expected to modify the catalytic properties of the prepared materials (Xia and al. [2]). The aim of this work is the comparative study of the activation of an alumina catalyst with both conventional calcination and a plasma-based system, in order to evaluate if the plasma treatment in a low pressure fluidized bed reactor is efficient to replace thermal calcination. Concerning the plasma process, the role of the plasma electrical discharge type, as well as the power density, was studied. The characterization of the catalysts, in order to understand the influence of plasma treatment on catalytic performances, is continuously in research. This comparison with “classical calcination" under air at different temperature was studied in order to evaluate eventual catalytic advantages of the plasma treatments.
The catalyst is Ag (2.5wt.%)/y-Al2O3 spheres, it was prepared by an excess impregnation method with a solution of silver nitrate (AgNO3). Then, the excess of solution was evaporated at 60°C under reduced pressure. Finally, the catalyst were dried, prior to the two different activation processes: (i) calcination under air flow at 500°C for 2 h (10°C.min‘l) in a fix-bed reactor or (ii) plasma treatment in a fluidized bed reactor, with a discharge microwave. In this last process, the impregnated powders were fluidized by an Ar gas or a mixture of Ar/O2 gas passing through a porous glass plate, the diameter sieved 600 pm in order to obtain a homogeneous fluidization. Thermogravimetric analyses (TGA) and derivative of loss of mass versus the time thermogram (TGD) were performed from Room Temperature (RT) up to 800°C in industrial air (100 cm’.min , 30 mg of catalyst).
In order to have a better understanding of the effect of the plasma activation, TGD were performed on three samples: (i) untreated and (ii) all plasma treated catalyst by M.W and (iii) calcined samples. The TGD curve shows exothermic peaks in the temperature range 200-550°C whereas the weight loss observed between 210°C and 500°C corresponds to loss of NO3 ligands. The purpose of the various treatments is to eliminate nitrates absorbed on the surface of catalysts to obtain a better catalytic activity. The TGD results, in the Figure la., indicate that calcination at 550°C has totally eliminated the ligands.
21

NOEA 2011
Zakopane 4-7 September 2011
Figure la. : TGD analysis of 2.5% silver on y-AfiOj spheres after various temperature of calcination : (X) 500°C-2h, (0) 400°C-2h, (A) 300°C-2h (D) 200°C-2h (O) 100°C-2h (») without treatment. Heating rate: IO°C/min, carrier gas: air, final temperature: 800°C
Figure lb. : TGD analysis of 2.5% silver on y-Al2O< spheres as a function of different microwave plasma treatments at various powers : (D) M.W-500Watts, (K) M.W-800Watts. And (X) calcination (500°C-2h), (•) without treatment. Heating rate: 10°C/min, carrier gas: air, final temperature: 800°C
In the Figure lb., we analyzed the various samples treated by microwave plasma, we followed the effect of the processing power plasma on the decomposition of nitrates. We notice that when the power increases to 800 Watts, it remains little of nitrate on the surface of catalyst. The increase in the power M.W plasma has a positive influence on the decomposition of nitrates, the less there are nitrates which desorbed. The plasma treatment with microwave at 500 Watts can be associated with a calcination of 400°C, and at 800 Watts, we admit that it has the same effect than a calcination at 500°C. During the study we also checked this effect on another support, zeolite. The results confirm those observed on this support presented. We also tested various catalysts treated by plasma and by calcination in order to compare their catalytic activity to NOX abatement in mobile sources.
11 ] A. Brockhaus, D. Korzec, F. Werner, Y. Yuan, J. Engemann, Surf. Coat. Technol. 74-75, (1995) 431
1. W. Xia, O.F.-K. Schluter, C. Liang, M.W.E. van den Berg, M. Guraya, M. Muhler, Catal. Today 102-103,(2005)34
2. M. Karches, M. Morstein, P. Rudolf von Rohr, R.L. Pozzo, J.L. Giombi, M.A. Baltanas, Catal. Today 72, (2002) 267
3. M. Karches, Ch. Bayer, Ph. Rudolf von Rohr, Surf. Coat. Technol. 116-119, (1999) 879
4. R. Jafari. M.Tatoulian, W. Morscheidt, F. Arefi-Khonsari, React. Fund. Polym. 66, (2006) 1757
22

NOEA20I1
Zakopane 4-7 September 2011
P03
##### State-of-the-art nitrogen oxide removal from off-gases of stationary sources by ammonia
##### M.A. BUZANOWSKI1
1 Peerless Mfg. Co., Dallas, TX, USA
Although selective catalytic reduction (SCR) of NOX is presently a mature technology, new design applications and stricter performance requirements present significant challenges and an urgent need for innovative technology development. This article discusses the state-ofthe-art design of commercial ammonia-based SCR systems designed for stationary sources. Particular attention is given to controlling NOx and ammonia slip emissions at ultra-low concentrations, new generation of exhaust systems for simple cycle power plants, improved ammonia injection grids, control systems designed for non-steady state operations, mathematical modeling of SCR systems designed for power plants and SCR catalyst poisoning.
Ammonia, or its precursor, is needed to reduce NO to innocuous nitrogen and water. One method of injecting ammonia into a flue gas flow utilizes an external ammonia vaporization system in which liquid ammonia (either in anhydrous or aqueous state) is vaporized in a vaporizer, utilizing hot air or flue gas, and then routed to a distnbution/injection grid for injection into flue gas at the location upstream of an SCR catalyst. A new arrangement of vaporizers used for efficient ammonia generation! 1] is compared for different SCR process configurations.
Further, this article presents recent efforts on improving the functionality of the ammonia injection grid (AIG)[2J. Computational and experimental studies performed on the AIG resulted in significant increases in the turbulence mixing between the injected ammonia and the exhaust flue gas. Improved mixing is instrumental to maximize catalyst performance, extend catalyst operating life, optimize catalyst volume, decrease system pressure drop, minimize reagent use and ammonia slip and reduce the overall size of the SCR system. Different arrangements of the AIGs[3],[4] developed to reduce deviations of the NH-/NO, ratio, temperature and flue gas flow are compared with conventional designs.
Considering control systems, many exhaust systems that use SCR technology for controlling emissions are designed to operate at the steady-state of the underlying combustion process. The facilities for which such exhaust systems are used typically operate in a steadystate condition. Therefore, the control schemes arc designed for the times at which the systems are operating most. One of the problems in the current control schemes for SCR processes is how to handle transient, non-steady-state conditions, e.g., start-up, shut-down, heavy-loading and unloading. In these transient conditions, the operating conditions cannot be assumed to be the same as in steady-state. Therefore, the SCR system will generally not operate as designed or will not achieve the expected steady-state performance as designed within a tight time tolerance.
The steady-state SCR process operates optimally when there is a unitary molar relationship between the input NOx and the injected ammonia concentration. If there is an imbalance of this molar relationship and locally, more ammonia than NOx is supplied, ammonia slip will be present. An imbalance is typical in actual operation of SCR systems. Therefore, ammonia slip is usually assumed to be present in such systems. It should be noted that, during startup transitions, the SCR process experiences continuous non-slcady-slate operation. The startup condition itself is a transient state or condition in the operation of the underlying process. However, the non-steady-state conditions that occur during startup, or most other transient states, are continuous. These transient startup conditions include parameters, such as low exhaust gas temperature, insufficient catalyst volume, abnormal levels of pollutants, and the rapid rate of change of these operating parameters, all play a role in the dynamics and effectiveness of the SCR process during such non-sleady-slate operations. New control technique has been proposed to maximize NOx removal efficiency during transient operations[5].
23

NOEA 2011
Zakopane 4-7 September 2011
An SCR system, when designed for a simple cycle turbine, presents a significant calculation and modeling challenge due to its compact design and stringent performance requirements. In particular, uniform flue gas velocity profiles, required by environmental catalysts installed in the ductwork of this system, must be met. Custom flow devices optimized for the turbine SCR systems and ductwork are required. This article discusses possible steps taken to ductwork internals.
Mal-distribution (non uniformity) in the velocity profile within a high efficiency SCR system is one of design considerations. With a specified velocity profile, high and low efficiency retrofits are compared. It is demonstrated that, while the slight mal-distribution in the velocity profile may significantly impact the performance of a high efficiency retrofit, it may be unnoticeable for low efficiency retrofits.
Finally, this paper discusses a new compact exhaust system and efficient arrangement of the tempering air system for simple cycle power plants[6]. The proposed system includes transitioning hot exhaust flue gas into pre-oxidation section of the exhaust system, passing hot exhaust gas through the oxidation catalyst for the CO emissions control, injecting tempering air stream into the post-oxidation section of the exhaust system, and passing cooled flue gas through the reduction catalyst for the NOx emissions control. The resultant benefit of this newly designed process|6] is a more effective use of catalysts and a smaller exhaust footprint.
1. M.A. Buzanowski, G. Smith, T. Shippy, Systems and methods for liquid vaporizers and operations thereof, US Patent Appl. US 20100029053
2. M.A. Buzanowski, P.J. Burlage, D.Z. Fadda, Reagent injection grid, US Patent 7,383,850, also Fluid mixing apparatus with injection lance, European Patent Appl. EP2248577 and EP1681089
3. M.A. Buzanowski, Control for ammonia slip in selective catalytic reduction, US Patent 7,166,262
4. M.A. Buzanowski, Ammonia distribution grid for selective catalytic reduction (SCR) system, US Patent Appl. US200040057888
5. M.A. Buzanowski, S.P. McMenamin, T. Shippy, Controlling ammonia flow in a selective catalytic reduction system during transient non-steady-state conditions, US Patent Appl. US20101001201
6. M.A. Buzanowski, S.P. McMenamin, Integrated exhaust gas cooling system and method, US Patent Appl. US20110158876
24

NOEA2011
Zakopane 4-7 September 2011
K04
##### Simultaneous NO reduction and soot oxidation on transition metal oxide catalysts
##### M, NAJBAR1, E. PAŁKOWSKA1, J. DUTKIEWICZ1,
##### I. NAZARCZUK1, L. LITYŃSKA-DOBRZYŃSKA2, E. BIELAŃSKA3, A. WESEŁUCHA-BIRCZYŃSKA1, W. ŁASOCHA1, J. CAMRA1, M. KOZICKI1
1 Faculty of Chemistry, Jagiellonian University, 3 Ingardena St., 30-060 Krakow, Poland,
e-mail: mnajbar@chemia, uj. edu.pl
Institute of Metallurgy and Materials Science Polish Academy of Sciences,
30-059 Cracow, 25 Reymonta St., Poland
Jerzy Haber Institute of Catalysis and Surface Chemistry,
Polish Academy of Sciences, 8 Niezapominajek St., 30-329 Kraków, Poland
Direct NO decomposition is the most desirable method to remove NOX from exhausts because the reaction is thermodynamically favorable and does not need any reducer.
The activity of the numerous catalysts in this reaction was checked. The precious metals [I] zeolites containing transition metal cations [2], transition metal oxides [3], transition metal oxides promoted by alkali or alkaline earth metal [4] and perovskites [5], were found to be effective.
It is well known that the direct NO decomposition is strongly diminished by an excess of oxygen present in off gases of the stationary sources of emission [6] as well as in exhaust of the Diesel engines [2], SO2 and H2O present in off-gases also affect catalyst activity in the direct NO decomposition [6]. The effect of such ingredients as hydrocarbons and CO is always considered to be beneficial.
Soot particles are another dangerous air pollutant. The interest of the direct decomposition of both, NO and soot, o the transition metal oxide catalysts [7-9] is still growing. Carbon is considered to be a real catalyst and transition metal oxide to be active in dissociative O2 adsorption. CC(O) surface complexes are formed on carbon surface by oxidation with O2 or NO2, independently on the presence of metal oxide. They decompose above 525K, yielding carbon oxides and free active sites. The role of the transition metal oxide is to transfer atomic oxygen to the soot surface and, thus, to enhance the CC(O) concentration.
Iron containing oxides were found to be effective catalysts in the direct NO and soot conversion [9],
In this presentation special attention will be given to the results obtained with the use of a Ee 2O3 - NiFe2O4 biphasic catalyst formed on the acid-resistant austenitic steel supports during their thermoprogrammed oxidation.
Publication co-financed by the European Regional Development Fund under the Innovate Economy Operational Programme 2007-2013, POIG.OI.01.02-12-112/09 project.
[ 1 ] D.D. Miller, S.S.C. Chuang, J.Phys. Chem. C 113 (2009) 14963, and references therein.
1. A.M. de Oliveira, I.Costilla, C. Gioia, I.M. Baibich, V.T. da Silva, S.B.C. Pergher, Catal. Lett. 136 (2010)185, and references therein.
2. SJ. Huang, A.B. Walters, M.A. Vanice, J. Catal. 192 (2000) 29, and references therein.
3. W.-J. Hong, S. Iwamoto, S. Hosokawa, K. Wada, H. Kanai, M. Inoue, J.Catal. 277 (2011) 208, and references therein.
4. J.J.Zhu, A. Thomas, Appl.Catal. B:Environ. 92 (2009) 225, and references therein.
5. R. Zhu, M. Guo, E Ouyang, Acta Phys. Chim. Sin. 24 (2008) 909, and references therein.
6. V. V. Lissianski, V. M. Zamansky, P. M. Maly, M. S. Sheldon, Combust. Flame 125:1310 (2001), and references therein.
7. R. Zhu, M. Guo, F. Ouyang, Catal. Today 139 (2008) 146, and references therein.
25

NOEA2011
Zakopane 4-7 September 2011
D. Reichert, H. Bockhom, S. Kureti, Applied Catalysis B: Environmental 80 (2008) 248, and references therein.

NOEA 2011
Zakopane 4-7 September 2011
C02
##### Modelling of structured reactor based on wire gauzes and zeolite catalyst for ammonia reduction of NOX from biogas turbines
##### P. JODŁOWSKI1, J. OCHOŃSKA13, D. Mc CLYMONT4, B. GIL1, A. KOŁODZIEJ23, S. KOŁACZKOWSKI4, J. ŁOJEWSKA1
1 Faculty of Chemistry, Jagiellonian University, 3 Ingardena St., 30-060 Kraków, Poland
2 Institute of Chemical Engineering of the Polish Academy of Sciences,
5 Bałtycka St., 44-100 Gliwice, Poland
Faculty of Civil Engineering, Opole University of Technology,
48 Katowicka St, 45-061 Opole, Poland
Department of Chemical Engineering, University of Bath,
Claverton Down, Bath BA2 7AY, UK
The current technological means for cleaning exhaust gases from gas turbines are based on two consecutively-working converters: the first for NOX reduction and the second for VOC combustion. However, they suffer from several major drawbacks, the most important of which are: the size of the system (more than 10 m long) and catalysts based on noble metals, both of which greatly increase the costs of the installations. The solution for the first problem is the application of short channel structures as reactor fillers, and for the second - the search for catalytic active nanostructures.
The aim of the paper is to design the wire gauze based structured reactor with the Cu2+ exchanged zeolite Y. This part of the study is devoted to modeling the mass transport of reactants through the assumed structures of wire gauzes. The structured catalytic reactors propose in this study expand the idea of monoliths, a successful widespread solution for vehicle exhaust removal, towards microstructures of short channels used as reactor fillers. The main advantage of structured catalytic reactors over the monoliths is that they show substantially higher mass and heat transport coefficients with reasonable pressure drop within the reactor [1-4], This is due to the fact that short channels of the elaborated geometry prevent laminar flow and facilitates reactants mixing, in contrast to long capillary channels of monoliths in which laminar flow fully develops.
In this study the reactor composed of a stack of 47 wire gauzes was used for modelling. The reactor length was 0.1 m, inlet temperature 573 K, and NO concentration 3000 ppm of a flow rate 2.66 m/s. The hydraulic diameter of the mesh was 3.29-1 O'4 m. The reaction kinetics (power type kinetic equation) was derived from the results of catalytic tests for NO reduction with NH3 in grandientless reactor. The reaction tests and the methods of preparation of the catalysts together with the physicochemical analyses are presented in the accompanying paper [5]. The reaction was assumed to be of a first order for the oxygen excess on the catalyst surface. The reactor model was based on 4 balance equations between the gas phase, catalyst surface and bulk .The mass transfer equation was obtained using the idea and the solutions presented by Kołodziej et al. [4] for the heat transport which was then transferred using Chilton Colburn analogy. The expansion of the previous approach was to include temperature as a variable in solving the balance equations which was hoped to refine the model considered before.
The exemplary results of the modeling are presented in Figure 1 for the kinetic data obtained from the literature [6] (kinf= 7.45 • IO9 m/s, Ea=85.9 kj/mol).
27

NOE A 2011
Zakopane 4-7 September 2011
Figure 1. Comparison of modeling mass and heat transfer results for the wire gauze reactor (L= 0.1 m, 4>= 0.1 tn) and the monolith (L= 0.1 m, <P= 0.1 m): A) axial surface temperature profile. B) axial hulk temperature profile, C) fractional conversion
The results obtained for wire gauzes are compared here with the monolith of the same length and channels diameter. As can be noted the wire gauze reactor has an advantage over the monolith allowing better heat and mass transfer throughout the reactor. This is demonstrated by even temperature profile in the wire gauze reactor for which surface and bulk temperature reach the same values shortly after passing the reactor entrance, unlike for the monolith in which we observe the temperature gradient along the reactor axis. The highest conversion can also be achieved in the wire gauze reactor at around 0.02 m from the reactor center which means that in comparison with the monolith the wire gauze reactor can be reduced by around 10 times.
11] A. Kołodziej. J. Łojewska, Microstructured Catalytic Reactor for VOC Combustion: Design, Evaluation and Examination, Chem. Eng. Proc. 46 (2007) 637
1. A. Kołodziej, J. Łojewska. Flow resistance of wire gauzes, American Institute of Chemical Engineers Journal AIChE J 55 (2009) 264
2. A. Kołodziej, J. Łojewska, Experimental and modelling study on flow resistance of wire gauzes, Chemical Engineering and Processing 48 (2009) 816
|4| A. Kołodziej, J. Łojewska, Mass transfer for woven and knitted wire gauze substrates: Experiments and modeling Catal. Today 147S (2009) SI20
1. A. Knapik, J. Ochońska, D. McClymont, A. Rogulska, P. Jodłowski, B. Gil. W. Makowski, A. Kołodziej, S. Kołaczkowski, .1. Łojewska, Copper exchanged zeolite in structured reactor based on wire gauzes for ammonia reduction of nitrogen oxides from biogas turbines, submitted to Catalysis Today (NOEQ 2011)
2. M.Koebel, M. Elsener Selective catalytic reduction of NO over commercial DeNOx-catalysts: experimental determination of kinetic and thermodynamic parameters. Chemical Engineering Science 53(1997)657-669
28

NOEA2011
Zakopane 4-7 September 2011
C03
##### Copper exchanged zeolite in structured reactor based on wire gauzes for ammonia reduction of nitrogen oxides from biogas turbines
##### J. OCHOŃSKA13 A. KNAPIK1, D. Mc CLYMONT4, A. ROGULSKA1-2, P. JODŁOWSKI1, B. GIL1, W. MAKOWSKI1, A. KOŁODZIEJ23, S. KOŁACZKOWSKI4, J. ŁOJEWSKA1
1 Faculty of Chemistry, Jagiellonian University, 3 Ingardena St., 30-060 Kraków, Poland
2 Institute of Chemical Engineering of the Polish Academy of Sciences,
Bałtycka St., 44-100 Gliwice, Poland
J Faculty of Civil Engineering, Opole University of Technology,
48 Katowicka St., 45-061 Opole, Poland
Department of Chemical Engineering, University of Bath,
Claverton Down, Bath BA2 7AY, UK
The motivation for this study arises from the opportunity to gasify renewable sources of biomass (e.g. forestry residue, farming residue, municipal waste), to obtain biogas (H2, CO, CO2, N2, HCs) which is used as a fuel in gas engines. Gas engines (turbines) producing electricity or hot water provide energy at a local level. A major challenge is to develop appropriate catalytic technology for the treatment of exhaust gases (from the engine), to meet the new European Waste Incineration Directive (WID) for this type of a process. Although the cleaning installations for VOC and NOx are known and work successfully in power stations there are several important problems typical of biogas exhaust. These include reduction of the size of cleaning installation, ammonia slip, thermal deactivation (hot spots) and catalyst based on nobel metals. The remedy can be the application of the so called structured reactors based on metallic short channel structures of enhanced mass and heal transport [1] that are able to considerably shorten the reactor length. The results of the optimisation of the reactor transport phenomena are presented in the accompanying paper [2]. The application of such structures is entirely dependent on the development of new, highly-active catalysts with an increased conversion adjusted to high transport properties and also the methods of catalyst layering on the metallic surface.
In line with the requirements stated by the structured reactors and the NH3-SCR process seem the copper-cxchanged zeolites, which are known for their remarkable activity both in in the nitrogen oxides reduction and also in direct NO decomposition [3,4]. For the latter, NH3 is activated on Brpnsted acid sites leading to NH4+ ions. Therefore the presence and correct strength of acidic OH groups is required. Use of steamed form of zeolite Y as a matrix for the copper cations should lead to the active catalyst, having both Cu+ and H+ cations embedded into microporous solid additionally containing mesopores, formed by steaming, facilitating reagents transport. Moreover, steaming process stabilized existing acidic centres, protecting them from further decomposition under harsh conditions of the catalytic reaction.
The Cu2+-Y zeolite was prepared for this study by exchanging the steamed form of NH/-Y zeolite (LZY-82, Linde of Si/Alfran) = 4.5) by three-fold ion exchange from aqueous solution of Cu(NO3)2 at 85°C.The sheeLs of kanthal steal were used as the catalyst carriers. The catalyst was deposited on the surface of the precalcined (IOOO°C) and washcoated (AI2O3 or TiO2) surface of the carriers by impregnation. Both forms of the zeolite catalyst: powder and deposited one were subjected to further analyses. The powder catalyst was examined by XRD, UV/VIS, Raman, SEM/EDX methods. The types of active centres present within the zeolite structure were checked by the in situ FTIR measurements of sorption and desorption of pyridine, NO and CO as probe molecules. The surface of the deposited catalysts was analysed with the standard SEM/EDX method to check the distribution of the material and the coupled system of AFM and confocal Raman microscope to check the structure, dispersion and the distribution of the material. The catalyst were tested in the reduction of NO2 with
29

NOEA201I
Zakopane 4-7 September 2011
ammonia in the gradientless reactor to derive kinetic parameters. The results allowed Tor the advanced correlations of the catalyst to establish fundamental structure-performance relationships.
1. A. Kołodziej, J. Łojewska, Catal. Today 147S (2009) S120
2. P. Jodłowski, J. Ochońska, D. McClymont, B. Gil, T. Łojewski, A. Kołodziej, S. Kołaczkowski, J. Łojewska, Modelling of structured reactor based on wire gauzes and zeolite catalyst for ammonia reduction of NOx from biogas turbine, submitted to Catalysis Today ((NOEQ 2011)
3. P. Pietrzyk, B. Gil, Z. Sojka, Catal. Today 126 (2007) 103-111
4. K. Sun, H. Xia, Z. Feng, R. Sanlen, E. Hensen, C. Li, J. Catal. 254 (2008) 383

NOEA2011
Zakopane 4-7 September 2011
P04
##### NOX removal from stationary sources by selective catalytic reduction
##### A. E. PALOMARES',
1 Institute de Tecnologia Quimica (U.P.V.-C.S.I.C.) Universidad Politecnica de Valencia,
Camino de Vera s.n. 46022-Valencia (Spain), apalomar@iqn.upv.es
NO, emissions are one of the main environmental concerns related with atmospheric pollution. The data from the Annual European Union LRTAP Convention emission inventory report show that in 2009, 9233.5 Gg of NO, were emited in the EU-27. Although the NO, emissions in the European Union have decreased in almost 40% since 1990, NOx emissions for the EU-27 as a whole are projected to be 6 percent above the aggregated Member State ceilings and 16 percent above the stricter ceiling for the European Community as a whole set for 2010. These emissions came mainly from road transport (around 45%) and from stationary industrial combustions (around 35%) and new processes to control this pollution are imperative. Among the technologies envisaged for NO, emission control, the most widely applied are the selective catalytic reduction of NO, by NH3 in stationary sources and the three way catalysts for the mobile sources. Both systems are commercial and efective but both present some problems. The former one requires the use of a pollutant gas such as ammonia, that makes the operation complicated. The last one gives excellent results when the air to fuel ratio is close to the stoichiometric ratio, but the efficiency diminishes in the presence of an excess of oxygen. Nowadays the tendency is to use engines with better fuel efficiency, that work under lean bum conditions, i.e. with an excess of oxygen over the stoichiometric ratio. These operation conditions strongly diminish the efficiency of the traditional three way catalysts, and for this reason, other alternatives as NSR catalysts or the NO selective catalytic reduction with urea are being implemented.
Regarding to the NO, emissions from stationary sources, the main sources are the public electricity and heat production (1780 Gg in 2008), the stationary combustion in manufacturing industries and construction (851 Gg in 2008) and the petroleum refining industry (154 Gg in 2008). At the moment the best available technologies (BAT) for the NOx emission control in these processes are based in the use of low-NO, burners or in the selective (catalytic or non catalytic) reduction with ammonia (or urea). The main problem of the selective reduction is the necessity of a NO/NH3 ratio of 1, with the possible spill of ammonium and the formation of corrosive salts in presence of SO2.
The catalyst used for the NOx selective catalytic reduction wtih ammonia are based in V2O5/TiO2 or more recently in metal exchanged zeolites. Other alternatives under research involve the catalytic decomposition of NO, using metal exchanged zeolites as catalysts. Unfortunately, the activity of these materials is strongly diminished by the presence of O2, water and SO2. Another approach involves the NO, selective catalytic reduction (SCR) with hydrocarbons in the presence of O2. This alternative has attracted much interest and it could be a promising way to remove nitrogen oxides. Nevertheless the application of this system requires active catalysts in a wide range of operation conditions and during extended time periods. In the last years main attention has been paid to the use of Cu/Co-ZSM5 or Cu/Co-beta as catalysts for the selective catalytic reduction of NO in presence of oxygen. Nevertheless no clear explanation has appeared about the mechanism of the reaction neither about the reason why these zeolite structures are active. Recently it has been found that in order to obtain an active catalyst based in Co-zeolites for the NOx SCR with hydrocarbons is necessary that the zeolite presents an adequate topology: medium size pores, a Si/AI ratio of 8-30 and the absence of big cavities. The cobalt must be ion exchanged, because if the metal is in the zeolite framework the active sites are not accessible to the reactants (Figure 1). In addition, for a commercial use of the catalyst, it has to be hydrothermically stable.
31

NOEA2011
Zakopane 4-7 September 2011
Figure 1. NOX conversion in C3Hg-SCR on different Co/zeolites (850 ppm NO, 550 ppm C3H8, 8% oxygen, N2 as effluent, T=723 K)
Another important source of NOx emissions are the fluid catalytic cracking units (FCCU). Current NOj control strategies for these units include (i) hydrotreating of the feed to minimize NOX precursors, (ii) flue gas treatment in a tail-end unit (iii) modification of the design or the operating conditions of the regenerator and (iv) the use of additives, which is probably the most simple and cost-effective method. This additive should operate at the FCC regenerator temperature (700-750“C), for this reason conventional DeNOx catalysts used for other processes can no be used in the FCC unit because its high temperature. Consequently there is an urgent need to develop new NOX catalytic reduction additives that are active in these conditions. Up to now different materials have been proposed for this purpose as Mg-Al mixed oxides derived from hydrotalcites with copper or cobalt that can simultaneously remove NOX and SO2, derivatives of MCM-36, perovskite based catalysts and Cu-Al/Ce-Al complex oxides, nevertheless more active materials are necessary. In this way clusters of Sn -Cu-Al-0 interacting with Ce-Al mixed oxides highly dispersed on the y-Al2O3 have been described as active catalyst in this reaction, because the strong interaction between the two complex oxides having an imperfect structure, stabilizes the active sites and provide an active catalyst for the NOx removal in presence of oxygen at high temperatures.
A revision of the different approaches for the NOx removal from different stationary sources by selective catalytic reduction will be presented.
1. R.M. Heck, Catal. Today 53 (1999) 519
2. M. Iwamoto, Stud. Surf. Sci. Catal. 130A (2000) 23
3. A.E. Palomares, F. Imbert, J.G. Prato, A. Corma, Appl. Catal. B 75 (2007) 88
4. A.E. Palomares, A. Uzcitegui, A. Corma, Topics in Cat. 52(8) (2009) 1060
32

NOEA 2011
Zakopane 4-7 September 2011
K05
#### Modified clay minerals as effective catalysts of the DeNOx process
#### L. CHMIELARZ1,
1 Faculty of Chemistry, Jagiellonian University, 3 Ingardena St., 30-060 Kraków, Poland
Clays are very interesting materials for catalysis and therefore various methods were proposed for their activation in catalytic processes. Large group of clay minerals can be relatively easy intercalated with metal oxide pillars (e.g. A12O3, TiO2, ZrO2), which increases their surface area and microporosity (Fig. 1). The obtained materials, called Pillared Interlayered Clays (PILCs), were reported to be effective catalysts of various processes, including DeNOx [e.g. 1].
Another way of clay minerals pillaring is based on the surfactant directed method using alkylammonium cations and neutral alkylamines as surfactants and cosurfactants, respectively and teraethylorthosilicate (TEOS) as silica source (Fig. 2). These relatively new materials, called Porous Clay Heteroctructures (PCHs), are characterized by high surface area, combined micro and mesoporous structure as well as high thermal stability [e.g. 2, 3].
33

NOEA2011
Zakopane 4-7 September 2011
Acid-modifications of clay minerals were also reported as an effective method for their catalytic activation [e.g. 4]. Acid-modifications of vermiculite and phlogopite resulted in partial leaching of cations (including iron ions) from octahedral sheets of clays and their deposition, in the form of separate cations or aggregates, on the particle surface. Additionally, acid-modifications significantly increased the specific surface area and porosity of the clay samples. Therefore, such easy and cheap method can result in activation of clay minerals for catalytic processes in which iron plays a role of an active component. Various types of clay minerals (montmorillonite, saponite, vermiculite) were used as raw materials for the preparation of pillared interlayered clays and porous clay heterostmctures. PILCs were produced by direct exchange of interlayer sodium cations in montmorillonite (sodium form) for aluminium (Al-PILC), titanium (Ti-PILC) or zirconium (Zr-PILC) oligocations. PCHs were obtained by the surfactant directed method. Tetraethylorthosilicate, titanium isopropoxide and aluminium isopropoxide were used as source of silica, titania and alumina, respectively. Three types of PCH materials were synthesized: silica (Si-PCH), silica-titania (Si-Ti-PCH) and silica-alumina (Si-AI-PCH) pillared clays. In the next step copper and iron were introduced to PILCs and PCHs by an ion exchange method.
A next series of catalysts was obtained by treatment of vermiculite with concentrated mineral acids (HNO3, HC1, H2SO4) for 2,8 or 24 hours.
The pillared clays as well as acid-activated vermiculites were characterized with respect to chemical composition (XRF, EPMA), structure (XRD, FT-IR), texture (BET), morphology (SEM), coordination and aggregation of transition metal species (UV-vis-DRS) and surface acidity (FT-IR). Finally, the clay samples were tested in the role of catalysts for the selective catalytic reduction of NO with ammonia (DeNOx). Modified clay minerals were found to be active and selective catalysts of the DeNOx process, however their catalytic performance depends both the type of raw clay used for catalyst preparation as well as procedure used for its modification. In a group of pillared clays the best results were obtained for Ti-PILC and Si-Ti-PCH doped with iron, which were found to be active and selective catalysts in a broad temperature range of 300-500°C and additionally, stable in the presence of water vapour and SO2.
Acid treatment of vermiculite resulted in its catalytic activation for the DeNOx process. The best results were obtained for the clay samples treated with HNO3. Activation effect is probably related to deposition of iron, leached from octahedral sheets of vermiculite, on the clay particle surface.
Figure 3. Examples of DeNOx tests Ti-PILC (A) and Si-Ti-PCH (B) samples
Author acknowledge the Polish Ministry of Science for financial support in the frame of project N N507 426939 and S&B Industrial Minerals GmbH for supplying of clay minerals.
34

NOEA 2011
Zakopane 4-7 September 2011
1. L. Chmiclarz, P. Kuśtrowski, M. Zbroja, A. Rafalska-Łasocha, B. Dudek, R. Dziembaj, Appl. Catal. B. 45 (2003) 103
2. A. Galameau, A. Barodawalla, T.J. Pinnavaia, Nature 374 (1995) 529
3. L. Chmiclarz, P. Kuśtrowski, Z. Piwowarska, B. Dudek, B. Gil, M. Michalik, Appl. Catal. B. 88 (2009)331
4. L. Chmiclarz, A. Kowalczyk, M. Michalik, B. Dudek, Z. Piwowarska, A. Matusiewicz, Appl. Clay Science 49 (2010) 156

NOEA 2011
Zakopane 4-7 September 2011
P05
##### Modified carbonaceous materials in DeNOx reaction
##### T. GRZYBEK1, J. KLINIK1, M. MOTAK1, B. SAMOJEDEN1
1 Faculty of Energy and Fuels, AGH-University of Science and Technology,
Al. A. Mickiewicza 30, 30-059 Kraków, Poland; e-mail: grzybek@agh.edu.pl
Environmentally friendly energy production is one of the most important issues in 2Is1 century, especially for countries basing mainly on hard coal or lignite as energy source. There are several possibilities of the reduction of NOx emissions, such as changes in the parameters of combustion process, types of burners, addition of ammonia to the boiler etc, however, the efficiency of these methods is not totally satisfactory. Currently only secondary methods, and especially selective catalytic reduction of NOX with ammonia, which is widely used in the EU for stationary sources, show satisfactorily high emission reduction (ca 80-98 %). Most often V2O5/WO3/TiO2 is applied as a catalyst [1] at temperatures between 300 and 450"C. However, as this catalyst is insufficiently active at temperatures below 300°C, new materials are searched. Moreover, vanadia is environmentally unfriendly and this may lead to problems with deactivated catalysts. An alternative could be catalysts based on activated carbon. In 1970 the DeSOx- DeNOx process was proposed, basing on activated carbon used as an adsorbent/catalyst in a moving bed - called Bergbau-Eorschung method, further developed as Mitsui method. However, the activity of unmodified activated carbons was also unstisfactory and thus several ways of improvements were proposed.
The subject of this work is the review of possibilities of activated carbon modifiactions, with special stress laid on treatment with N-containing compounds [1-12], Several such compounds were used and different modification procedures applied, leading to a considerable increase both in activity and stability of the systems. They will be discussed in detail during presentation, while here only selected examples are given.
Modification procedures
Activated carbons are flexible systems, in which both textural and surface properties may be modified. Fig.I. summarizes typical treatments: oxidation either with gaseous or liquid media, high-, medium- or low-temperature modfication with N-containing species, and promotion with precursors of transition metal oxides/hydroxides. Such modification steps were used either separately or in series [e.g. I-12|.
Figure 1. The procedures of modification of DeNOx catalysts based on activated carbons
37

NOEA2011
Zakopane 4-7 September 2011
Catalysts prepared by all above mentioned methods were tested in DeNOx reaction at low-to-medium temperature region, between 120 and 300°C [e.g.1-12].
For activated carbons modified by oxidation and/or promotion with transition-mclal-oxide precursors, the following conclusions were made:
- oxidation increased NO conversion to the extent depending on the type of oxidant. Solutions of oxidizing compounds were more efficient than O2-containing mixtures. Aqueous solutions of HNOj proved the best.
- Several transition metal oxides, such as Mn, V, Fe, Co, Ni, Cu etc., were reported to improve DeNOx properties of activated carbons [e.g. 2,5]. It was necessary, however, to precede Me-introduction step with oxidation. The effect was explained by differences of MeOx distribution induced by the formation of oxygen-conlaining surface species prior to promotion.
The interest has focused lately on the introduction of nitrogen species into carbonaceous materials. Two main procedures were proposed: either the application of N-containing precursors such as appropriate polymers e.g.polyacrylonitrile, followed by steps typical for activated carbon preparation (i.e. carbonization and activation), or post-treatment of activated carbon with N-containing species. In one of the first articles, Singoredjo et al showed that both methods led to the improvement of DeNOx properties, to an extent strongly dependent on the type of N-species [9]. During the last 10 years, mainly urea and ammonia, alone or in the mixtures with air were studied [ 1,6,7, 10-12],
The following parameters of the procedures were tested:
- the influence of pre-oxidation of activated carbons,
- high- vs medium-or low-temperature procedures (pure NH3 al ca. 800°C, NH3-air mixtures at medium temperatures from ca. 300 to 500°C, treatment with aqueous urea solutions (wet impregnation), followed by curing in air etc)
- the introduction of transition metal precursors (Fe, Mn) on N-trealed cabon materials. Fig.2. shows as an example the DeNOx performance of activated carbons treated with urea, ammonia or ammonia-air mixtures in comparison to nonmodified AC.
38

NOEA2011
Zakopane 4-7 September 2011
Figure 2. DeNOx properties of carbonaceous
N-compounds: NO conversion, N2O and CO2 formation
materials non-modified and modified with
The main conlusion from Fig.2 and similar data from literature is that treatment with N-species may lead to considerable improvement in DeNOx performance in low-to-medium temperature range. NO conversion was found to increase and N2O formation to decrease for so-modified samples. Simultaneously, stability towards oxidation increased. However, preparation procedure must be optimized, taking into account the pretreatment (oxidation) and appropriate choice of N-compound (or its mixture with air) and temperature of treatment. Pre-oxidation was, similarly as in case of promotion with transition metal oxides/hydroxides, of advantage. Urea treatment or ammoxidation at medium temperatures resulted in catalysts more active at lower temperatures than in case of high-temperature ammonia treatment [e.g. 1,12],
The performance of AC-ox-N may be additionally improved by the promotion with transition metal oxides/hydroxides, as it was successfully proven for MnOx [I] and FeOx.
The influence of H2() on catalytic performance
Only a few articles considered the influence of H2O on the DeNOx performance of cabonaceous materials [e.g. 7,12], For N-modifted carbonaceous materials, the presence of water led to the decrease in NO conversion, although the effect was smaller at higher temperatures. On the other hand, activated carbons modifed with N-species and MnOx showed considerable increase in selectivity to N2 [12], The effect is believed to be connected adsorption/desorption equilibrium of NO and/or NO2 , although literature information is not consistent.
Mechanistic considerations
Experimental results and literature discussions led to the more-or-less consistent mechanism of DeNOx reaction for a mixture without water for carbonaceous materials either unpromoted or promoted with MeOx. The route in dry stream is believed to take place through adsorption of NO on oxygen containing surface species (hence positive influence of oxidative treatment), oxidation of NO to NO2, sorption of ammonia as NH4+ or NH2 and decomposition of surface intermediates (NH4NO2 or NH2NO2)
39

NOEA201I
Zakopane 4-7 September 2011
to nitrogen and water. The promotion with transition metal oxides/hydroxides was proven to increase the number of acidic sites and thus NH3 adsorption [1]. It most probably also enhances NO oxidation rate.
It was observed that the formation of N2O was higher for active components with more pronounced redox properties [ I ]. Thus, it would follow that these are primary sites for ammonia oxidation.
The “dry route” for N-modified carbonaceous materials has not yet been established without doubt. There are some indications that the introduction of N-containing surface species which are basic in character, may lead to increased adsorption of very weakly acidic NO, this being the source of improvement observed in DeNOx. The matter is, however, far from being solved.
The role of water also needs additional information. Some experimental data indicate that the decrease in NO conversion, which is smaller for activated carbons than other catalysts, is a net effect of the increase in NO adsorption caused by N-surface groups and the decrease caused by the competition for these sites of NO and H2O. The improvement in selectivity, on the other hand, is believed to arise from the competition of H2O and NH3 for MeOx sites which leads to the decrease of the overabundance of labile oxygen on the surface.
Carbonaceous materials are promising catalysts for low-temperature DeNOx process. Of those, N-modified activated carbons show the best properties, the increased NO conversion, decreased N2O formation and increased stability towards oxidation. However, in order to prepare a successful catalyst, certain steps in the modification procedure are necessary, the most important of them being an oxidative pre-treatment. H2O influences DeNOx performance to a smaller extent than is usual for other catalysts. Moreover, with certain compositions and temperatures, NO conversions did not suffer too much while simultaneously a considerable decrease in selectivity to N2O was observed.
The mechanism of DeNOx on activated carbons has only partially been explained. The role of N-species is, as yet, not clear. The role of H2O also needs some more experimental information.
Acknowledgements: The work was supported by grant no. AGH 11.11.210.213.
[ 1 ] T. Grzybek, J. Klinik, M. Motak, H. Papp, Catal. Today. 137 (2008) 235
1. T. Grzybek, J. Klinik, M. Rogóż, H. Papp, Phys. chem. Chem. Phys. 1 (1999) 341
2. G. Marban G., A. B. Fuerte, Appl Catal. B. 55 (2001) 34
3. Z. Zhu, Z. Liu, S. Liu, H. Niu, T. Hu, T. Liu, Y. Xie, Appl. Catal. B. 26 (2000) 25
4. T. Grzybek, H. Papp, Appl. Catal. B 1 (4) (1992) 271
5. G. Szymański, T. Grzybek, H. Papp, Catal. Today. 90 (2004) 51
6. J. Muniz, G. Marban, A. B. Fuertes, Appl.Catal. B. 27 (2000) 2000
7. H. Teng, Y.-T. Tu, Y.-Ch. Lai, Ch.-Ch. Lin, Carbon 39 (2001) 575
8. L. Singoredjo, F. Kapleijn, J. A. Moulijn, J. M. Martinez-Martinez, H. P. Boehm, Carbon. 31 (1993) 213
9. T. Grzybek, J. Klinik, B. Samojeden, V. Suprun, H. Papp, Catal. Today. 137 (2008) 228
10. G. Marban, J. Muńiz, A. B. Fuertes, Appl. Catal. B. 23 (1999) 25
11. J. Klinik, B. Samojeden, T. Grzybek, W. Suprun, H. Papp, Nitrogen promoted activated carbons as DeNOx catalysts.2. The influence of water on catalytic performance, Catalysis Today (2011), doi: 1.1016/j.catlod.2010.12.009
40

NOEA2011
Zakopane 4-7 September 2011
K06
##### HC SCR as alternative process for NOx abatement in stationary and mobile sources
##### P. Da COSTA1
UPMC, Universite Paris 6, Institut Jean Le Rond d'Alembert,
CNRS UMR 7190,2 place de la gare de ceinture, 78210 Saint Cyr I’Ecole
Combustion of hydrocarbons (HC), as source of energy, causes environmental pollution. Theoretically, the products of this combustion are carbon dioxide and water. Nevertheless, the non-ideality of this reaction in the combustion chamber leads to the formation of a large number of pollutants. Among them, nitrogen oxides (NOX) are not only harmful for human beings but also contribute to environmental pollution by formation of acid rains, thus increasing the green-house effect and participating in the formation of photochemical smog. Thus, emission of NO, (NO + NO2) from vehicles and stationary sources are responsible for serious environmental problems.
The deNOx or NOx reduction is the specific post-treatment for the reduction of nitrogen oxides present in the exhaust streams in lean-bum conditions.
Nowadays, only NH3 SCR leads to high efficiency for NOx abatement both in stationary and mobile sources. For environmental reasons, it would be good to use only the pollutants present in the exhaust gases for the NOx reduction.
Thus, the SCR of NOX by methane can be a very attractive technology for the decreasing of NOX from stationary sources, because natural gas (methane) is readily available. Initially, Li and Armor [1] found that the most active catalysts for NOX removal by methane in oxygen excess were based on cobalt supported on several zeolites. Bimetallic cobalt and palladium loaded zeolites exhibited much more resistance to waler vapor than monometallic Co-zeolites [2]. Although they are more resistant, these catalysts also deactivate under long-term hydrothermal conditions. Another main obstacle of SCR of NO by methane is the low selectivity between the reaction with NO and O2 [3] and [4], This obstacle is important in the case of Pd, since Pd is very active for total oxidation of methane [5], The used of Pd supported on acidic materials such as zeolites for he SCR of NOX by methane, is correlated with the stabilization of the Pd2+ ions on acidic materials, which have low activity for methane oxidation [6], Therefore, other acidic materials have been tested, such as sulphated zirconia and sulphated alumina [7], Recently, a general three-function model for deNOx catalysis [8] was also proposed for metals in cationic form. The authors claimed that three functions are necessary for the deNOx process to occur: (i) oxidation of NO to NO2; (ii) mild oxidation of methane to alcohol and aldehyde, in the presence of NO2; (iii) reduction of NO to N2, assisted by the deep oxidation of the alcohol and aldehyde to CO2. Moreover, many authors report that H2 which is present in exhaust gases, is a very effective reducing agent under lean conditions [9].
In mobile sources, the situation is more complicated since the temperature of exhaust gases is not fixed and since the range of temperature of exhaust gases goes from RT to 350°C, thus the catalysts used for stationary sources cannot be used for mobile sources. In such processes, one hydrocarbon is still promising to reduce NOx: the ethanol. Thus, among the different active phases studied for NO x reduction, alumina supported silver-based catalysts have shown good results using either hydrocarbons or oxygenated compounds as reducing agents 110], Since precursory work of Miyadera and Koshida [11] on this catalytic system, many studies dealing with the characterization of silver particles have been performed [12], It is generally believed that cationic silver is predominant for low loaded catalysts, whereas metallic particles prevail when the silver loading is important [13]. Furthermore, oxidized silver state can refer to different silver species, while different oxidized silver species such as isolated Ag+ cations [14], Ag m n+ clusters [15], and silver aluminate AgA102 [16] have been observed. However, any agreement on the nature of the silver active species active for the reaction of NOX reduction has not been achieved yet
41

NOEA 2011
Zakopane 4-7 September 2011
which let us to think that the process is not mature yet but could be improved since the used materials will be well characterized.
[ 1 ] Y. Li and J. Armor, J. Catal. 150 (1994) 376
1. L.E Cordoba, G.A. Fuentes and C. Montes de Correa, Micropor. Mesopor. Mater. 77 (2005)
2. M. Iwamoto and H. Yahiro, Catal. Today 22 (1994) 5
3. M. Iwamoto and H. Hamada, Catal. Today 10 (1991) 57
4. CJ. Loughran and D.E. Resasco, Appl. Catal. B 7 (1995) 113
5. Y.-H. Chin, A. Pisanu, L. Serventi, W.E. Alvarez and D.E. Resasco, Catal. Today 54 (1999) 419
6. N. Li, A. Wang, L. Ren, M. Zheng, X. Wang and T. Zhang, Top. Catal. 30/31 (2004) 103
7. G. Djega-Mariadassou and M. Boudart, J. Calal. 216 (2003) 89
8. R. Marques, L. Mazri, S. Da Costa, F. Delacroix, G. Djega-Mariadassou and P. Da Costa, Catal. Today 119 (2007) 166
9. S. Kameoka, Y. Ukisu, T. Miyadera, Phys Chem. Chem. Phys. 2 (2000) 367
10. T. Miyadera ,K. Koshida, Chem. Lett. 1483 (1993) 1
11. A. Musi, P. Massiani, D. Brouri, J.-M. Trichard and P. Da Costa, Calal. Let. 128 (2009) 25
12. FC. Meunier, R. Ukropec, C. Stapleton, JRH. Ross, Appl. Catal. B 30 (2001) 163
13. K-I. Shimizu, J. Shibata, H. Yoshida, A. Satsuma, T. Hattori, Appl. Catal. B 30 (2001) 151
14. IH . Son, MC. Kim, HL. Koh, KL. Kim, Catal. Lett. 75 (2001) 191
15. N. Bogdanchikova, FC. Meunier, M. Avalos-Borja, JP. Breen, A. Pestryakov, Appl. Catal. B 26 (2002) 287
42

NOEA2011
Zakopane 4-7 September 2011
K07
##### Effect of Ci and C2 organic reducing agents on selective catalytic reduction of NO on FeSiBEA and CoSiBEA zeolites
##### J. JANAS*, W. ROJEK1, S. DŹWIGAJ2*
1 Institute of Catalysis and Surface Chemistry, Polish Academy of Science,
8 Niezapominajek St., 30-239 Krakow, Poland
Laboratoire de Reactivite de Surface, UPMC, CNRS,
UMR 7197, 3 rue Galilee, 94200 Ivry-sur-Seine, France
★Corresponding author: stanislaw.dzwigaj@upmc.fr
Recently [1,2|, we were reported that cobalt and iron containing BEA zeolites obtained by two-step postsynlhcsis method were active in selective catalytic reduction (SCR) of NO by ethanol. Their catalytic activity was strongly depended on the state of cobalt and iron introduced into the zeolite. It was found that CoSiBEA and FeSiBEA zeolites with cobalt and iron incorporated in framework zeolite as isolated tetrahedral Co(ll) and Fe(lll) species were the most active sites in this reaction.
For the present work, the CoojSiBEA and Fco.9SiBEA zeolites containing only isolated tetrahedral Co(II) and Fe(III), respectively, were prepared as a potential catalyst for SCR of NO by methane, methanol, ethylene and ethanol used as C| and C2 organic reducing agents.
Coo.7SiBEA and Fe^SiBEA zeolites (with 0.7 and 0.9 wt % of Co and Fe) were prepared by the two-step postsynthesis method described earlier [3-5] using an aqueous solution of Co(NO3)2 6 H2O and Fe(NO3)3'9 H2O at pH = 2.6 as cobalt and iron precursor and characterized by different physicochemical techniques: XRD, diffuse reflectance (DR) UV-vis, TPR, XPS and FTIR. The catalytic activity was examined in a conventional flow reactor coupled to an analytical system. The composition of the feed was: 1000 ppm NO, 1000 ppm of ethanol or ethylene, 2000 ppm of methane or methanol, 2 O2 vol. % with a catalyst volume 1 ml and GHSV (gas hours space velocity) 10,000 h *. Before catalytic tests, the samples were healed up to 523 K in oxygen/helium mixture and then NO and/or organic reducing agent vapour streams were switched on. The standard conditions were: 1 h catalytic runs at 523-773 K and (NO, and CO, concentrations al the reactor outlet were continuously monitored for checking if pseudo steady-state conditions were established).
The reaction temperature was increased every 50 K intervals up to 773 K, and then lowered in the same manner to 523 K in order to obtain a reproducible activity.
The presence of framework isolated tetrahedral Co(II) and Fe(III) in Co0.7SiBEA and Feo.<>SiBEA zeolites, respectively, is evidenced by DR UV-vis, XPS and TPR. These zeolites are much more active in SCR of NO by C2 reducing agent (ethanol and ethylene) than by C| reducing agent (methanol and methane). In Figure I we show, as an example, the NO conversion and N2 selectivity in SCR of NO by different reducing agents on Coo7SiBEA zeolite. These results show that catalytic activity of Coo.7SiBEA zeolite strongly depends on the kind of organic compound use as reducing agent. The catalytic activity are similar in the presence of ethanol and ethylene, with selectivity toward N2 exceeding 90 % for NO conversion from 30 to 55 % in the temperature range of 550-750 K and is much lower in the presence of methanol and methane with selectivity toward N2 about 15 - 20 % for NO conversion from 10 to 20 %.
A comparison of the NO conversion values in the SCR and NO oxidation reaction (without reducing agents) reveals that the activity in (he SCR reaction on both CoojSiBEA and Fe^SiBEA catalysts was higher than in the oxidation reaction.
43

NOEA 2011
Zakopane 4-7 September 2011
Figure I. NO conversion and N: selectivity in SCR of NO by methane, methanol, ethylene and ethanol on Coll 7SiBEA and Fe0,ySiBEA catalysts.
A comparison of the NO conversion values in the SCR and NO oxidation reaction (without reducing agents) reveals that the activity in the SCR reaction on both Co07SiBEA and Feo.9SiBEA catalysts was higher than in the oxidation reaction.
In conclusion, CoojSiBEA and Fe()<)SiBEA zeolites containing only isolated tetrahedral Co(II) and Fe(IlI) are very active catalysts in the SCR of NO by ethanol and ethylene. In contrast, both zeolites are much less active in the SCR of NO by methanol and methane. It is probably due to the formation of different kinds of the reaction intermediates in the presence of C and C2 reducing agents.
[ 1 ] J. Janas, T. Machcj, J. Gurgul, R.P. Socha, M. Che, S. Dźwigaj, Appl. Catal. B 75 (2007) 239
1. J. Janas, J. Gurgul, R.P. Socha, T. Shishido, M. Che, S. Dźwigaj, Appl. Catal. B 91 (2009) 113
2. S. Dźwigaj, M.J. Peltre, P. Massiani, A. Davidson, M. Che, T. Sen. S. Sivasanker, Chem. Commun. (1998)87
3. S. Dźwigaj, P. Massiani, A. Davidson, M. Che, J. Mol. Catal. 155 (2000) 169
4. M. Anpo, S. Dźwigaj, M. Che, Adv. Catal. 52 (2009) 1
44

NOEA2011
Zakopane 4-7 September 2011
K08
##### DeNOx assisted by hydrocarbons
##### A. AISSAT1,2, D. COURCOT1’2, S. SIFFERT1,2
1 Univ Lille Nord de France, F-59000 Lille, France
2 ULCO, UCEIV, F-59140 Dunkerque, France,
siffert@univ-littoral.fr, Tel.: +33-328658256 (S. Siffert)
Large quantities of pollutants to the environment are released from the combustion of biomass and fossil fuels. Among these contaminants are the nitrogen oxides (NOX) which are the source of severe environmental problems.
Research in the Held of NOX abatement has grown significantly in the last two decades. The general trend has been to develop new catalysts with complex materials in order to meet the stringent environmental regulations. Nowadays two main methods for the removal of NOX from emission gases are employed: the selective catalytic reduction of NOX with NH3 (SCR) which is applied for stationary sources such as power plants and the three ways catalyst (TWC) used for mobile sources such as automobiles. In spite of the intense research, these are only partial solutions and include serious drawbacks. Alternatively selective catalytic reduction of NOX using hydrocarbons as reductant (HC-SCR) is currently attracting a great deal of interest.
The aim of this review study is to gain knowledge on the selective catalytic reduction of NOX with hydrocarbons with the final goal to contribute to the development of suitable catalysts for NOX abatement. This review discusses briefly about the different sources and the emission levels of NOX, their influence on the environment and public health, their regulation, the approaches for their removal and the state of the art with respect to catalytic solutions for their removal is reviewed. Emphasis is placed on the selective catalytic reduction of NOX using hydrocarbons.
Selective catalytic reduction of NOX in the presence of hydrocarbons
Due to the drawback concerning NH3-SCR, as the escaping in the exhaust and its transportation and storage, SCR of NOX by hydrocarbons is believed to be the most promising way to eliminate nitrogen oxide. The main advantage of the corresponding reaction is the use of a gas mixture very similar to that found in exhausts [1],
In this review, several parameters of the SCR of NOX studied in literature are explored: the types of solids used in this reaction (metal ion-exchanged zeolite, supported metals, supported metal oxides) by exploiting also the nature of the active phase used, the catalytic stability of the materials and the mechanisms.
For illustration, the first catalyst that was found to have a good hydrocarbon NOX reduction capability in oxygen rich conditions was Cu/ZSM-5 [2-4], They showed that the catalytic activity of Cu-ZSM-5 could be greatly enhanced by small amounts of hydrocarbons in the presence of excess oxygen.
This reaction has been extensively studied over different cation exchanged zeolites [5] and over different base oxides (A12O3, TiO2, ZrO2, MgO) and these oxides promoted by Co, Ni, Cu, Fe etc. [6], However, many of these catalysts are deactivated in presence of water vapour [1], Forwards, another system Ag/y-AI2O3 catalyst was found to be active for HC-SCR [7,8] but much higher temperatures are required.
The presence of a small amount of hydrogen in the feed improved the catalytic activity significantly [9], H2 promotes the NO, reduction over Ag/y-AI2O3 catalysts when using a range of lower alkanes and alkenes and higher alkanes [10] as reductants. Silver has also been used in zeolites for HC-SCR of NOX with various reducing agents [11-14], Recently, Aissat et al. [15] studied to the role of toluene but also the presence of carbonaceous particles on the NOx reduction. A maximum of NOX reduction was also found during light off curve of hydrocarbon oxidation [15,16].
45

NOEA 2011
Zakopane 4-7 September 2011
In conclusion, the interest of the scientific community for this topic is reflected by the number of patents and contributions in the literature.
1. V.I. Parvulescu, P. Grange, B. Delmon, Catal. Today 46 (1998) 233
2. M. Iwamoto, H. Hamada, Catal. Today 10 (1991) 57
3. M. Iwamoto, H. Yahiro, K. Tanda, N. Mizuno, Y. Mine, S. Kagawa, J. Phys. Chem. 95 (1991) 3727
4. G.P. Ansell, A.F. Diwell, S.E. Golunski, J.W. Hayes, R.R. Rajaram, TJ. Truex, A.P. Walker, Appl. Catal. B 2 (1993) 81
5. E.A. Lombardo, G.A. Sill, J.L. d’Itri, W.K. Hall, J. Catal. 173 (1998) 440
6. R. Burch, J.P. Breen, F.C. Meunier, Appl. Catal. B 39 (2002) 283
7. T. Miyadera, Appl. Catal. B 2 (1993) 199
8. T. Miyadera, Appl. Catal. B 13 (1997) 157
9. S. Satokawa, Chem. Lett. 3 (2000) 294
10. M. Richter, R. Fricke, R. Eckelt, Catal. Letters 94 (2004) 115
11. J. Shibata, K. Shimizu, Y. Takada, A. Shichi, H. Yoshida, S. Satokawa, A. Satsuma, T. Hattori, J. Catal. 227 (2004) 367
12. J. Shibata, Y. Takada, A. Shichi, S. Satokawa, A. Satsuma, T. Hattori, Appl. Catal. B 54 (2004) 137
13. S. Satokawa, J. Shibata, K. Shimizu, A. Satsuma, T. Hattori, T. Kojima, Chem. Eng. Sci. 62 (2007) 5335
14. K. Shimizu, M. Hashimoto, J. Shibata, T. Hattori, A. Satsuma, Catal. Today 126 (2007) 266
15. A. Aissat, S. Siffert, D. Courcot, R. Cousin, A. Aboukai's, C.R. Chimie 13 (2010) 515
16. A. Aissat, D. Courcot, R. Cousin, S. Siffert, Catal. Today DOI: 10.1016/j.cattod.2011.01.033 (2011)
46

NOEA20I1
Zakopane 4-7 September 2011
K09
##### Influence of the crystallite size of nobel metals on the course of the DENOX reaction
##### D. NAZIMEK1, W. ĆWIKŁA-BUNDYRA1
1 University of Maria Curie -Skłodowska, Faculty of Chemistry,
Department of the Enviromental Protection, 20-031 Lublin,
M.Curie-Sktodowska Square, Poland
Catalysis is one the most important fields in industry where small particles are applied. An extensive treatment of particle size effects in catalysis has recently published [1]. An effect of the metal crystallite size in the SCR process has been investigated for rhodium and platinum [2,3]. Kinetic analysis done by Oh [4] suggests that the rate-controlling step may shift from the low-temperature N2/N2O formation path to the high-temperature N2 formation path with an increaese in the catalyst temperature. The present paper reports the effects of Pt, Rh, Pd and Ru dispersion on the course of the reaction between nitric oxide and carbon monoxide.
Catalysts.
The investigated catalysts M/AI2O3 was supported by y-AI2O3 obtained by classical impregnation method of the alumina supports by metal salts solution respectively and double impregnation of the alumina supports EDTA aqueous solution, following by metal salts solution respectively, [5], All obtained catalysts were reduced with hydrogen al 873K for 1 hour. The metals loadings were measured by X-ray fluorescence (XRE).
Methods.
Mean metal crystallite size was determined by X-ray diffraction (XRD) (occurance ± 30%) and from chemisorption measurements. Total surface areas of the catalysts examined were determined from argon adsorption at liquid nitrogen temperature by the BET method in a volumetric appartus ensuring a vacuum of al least 10'5 mm Hg. The same appartus was used for the determination of active surface areas of the reduced catalysts. The measurement of the activity and selectivity of the DENOX reaction was carried out in a gradientless reactor described in paper [6], All kinetic experiments were carried out in an atmosphere of helium and NO(1500 ppm) and C0(4500 ppm), determining the relationship between the reaction rate and temperature of this process. The reaction products were analyzed IR method and gas chromatography metod.
The authors of papers [7-10], has been found a special role of B5 sites existing on the metal surface area, in catalysis by metals in hydrogenolysis of alkane. The concentration of B5 sites (calculated data) reaches a clear maximum in the different interval crystallite size of Pt, Rh, Pd and Ru. The increase in the Pt crystallites size induced an increase reaction rate of NO conversion and increase selectivity towards N2O. In the case of rhodium catalysts, the reaction rate and selecticiy towards N2O show a clear maximum as a function of the crystallites size of rhodium. However, that the only Rh, Pd and Ru catalysts was found correlation between number of B5 sites for existing on the metal surface and selectivity reaction of DENOX towards N2O. The observed maximum of the reaction rate conversion of NO and selectivity towards N2O in the interval of Rh, Pd and Ru crystallite size is probably correlated with a concentration of low-coordination centers on the rhodium surface (probably B5 sites). Probably B5 sites may play a special role in the in the DENOX reaction by disociative chemisorption of NO on this site of active centers (including of B5 sites). 1 2 3 4
[1]	M. Che, C.O. Bennett, Adv. Catal. 36 (1989) 55
[2]	K. C. Taylor, Catal. Rev. - Sci. Eng. 35 (1993) 457
[3]	K. C. Taylor, Sciences and Technology, vol. 5, Springer-Verlag, Berlin, 1984
[4]	S. H. Oh, C. C. Eickel, J.Catal. 128(1991)526
47

NOEA20I1
Zakopane 4-7 September 2011
1. J. Barcicki, D. Nazimek, W. Grzegorczyk, T. Borowiecki, R. Erąk, M. Pielach, React. Kinet.Calal. Lett. 17(1981) 169
2. D. Nazimek, M. Kuśmierz, P. Kirszensztejn, P. J. Apllied Chem. 50 (2006) 41
3. D. Nazimek, J. Ryczkowski, React. Kinel. Catal. Lett. 40 (1990) 145
4. D. Nazimek, Appl.Catal. 12(1984) 227
5. J. R. Anderson, Sci. Prog. Oxf. 69 (1989) 461
6. D. Nazimek, J. Ryczkowski, Stud. Surf. Sci. and Catal. 119(1998)623

NOEA201I
Zakopane 4-7 September 2011
KIO
##### Structural-functional design of catalysts for gas emissions purification from nitrogen (I), (U) oxides
##### S. ORLYK1, S. SOLOVIEV1, T. BOICHUK1, P. KIRIENKO1
1 LV.Pisarzhevsky Institute of Physical Chemistry of the NAS of Ukraine,
31 Prosp. Nauky, 03028 Kyiv, Ukraine, orlyk@inphyschem-nas.kiev.ua
Issue of nitrogen oxides NxOy (NOX and N2O), one of the most dangerous pollutant the atmospheres, causing a hotbed effect, has reached 30 million ton in a year, and the most part from them has an anthropogenous origin. For last decade speed of allocation in atmosphere N2O has considerably grown. For neutralization of diluted exhaust gases (<l % N2O) in manufacture of nitric acid and processes of solid fuels combustion the N2O reduction by CO or CH (SCR-process for the nitrous gases containing oxygen) is perspective. The literature analysis shows, that the critical factor in design of catalysts of N2O decomposition (of "tail" gases) is reduction of influence of oxidizers (NO, SO2, O2, H2O) [I]. Thus, the problem of nitrogen oxides removal from oxygen-containing gas emissions both mobile, and stationary sources remains unresolved, and in the case of SCR-process application (CH and CO) is complicated by negative influence on the catalysts of a moisture and sulfur compounds. In this work results of slructurally-functional design of coball-containing catalysts for processes DeNOx, DeN2O, simultaneous conversion of N2O and NO in the gas mixes containing oxygen, H2O and SO2 are presented.
The preparation of the catalyst samples was described in [2], The catalytic activity of the samples was characterized by the conversion of N2O and NO into nitrogen and was determined in a flow system with a gradicnlless quartz reactor at atmospheric pressure at 250-550°C. The following reaction mixtures were used (vol. %): 0.2-0.5 N2O, 0.1-0.2 C3H8-C4HIO (2:1), 0.05-0.5 CH4 or 0.5-0.6 CO and 0.1-0.25 NO (2.5-5.0 O2), remainder He (or Ar) with GHSV= 6,000-12,000 h-1. In some experiments H2O (up to 2.6 vol. %) and SO2 (up to 0.2 vol. %) were added. The sample (fraction 1-3 mm) was roasted prior to testing at 550 °C for 1 h. The analysis of reagents and reaction products has been performed by a chromatographic method on molecular sieves of CaA (N2, NO, CO, O2) and Polysorb-1 (N2O, CO2). In the presence of excess oxygen (in the conditions of SCR-process) NO has been analysed by means of gas analyzer 344 KhL-04 (chemiluminescent detector).
In Tab.l the results of influence of the carrier nature on the activity of NO selective reduction by methane including in the presence of SO2 and H2O are submitted. The activity of Co-In-oxide catalysts depends of the carrier nature and the method of active component application, herewith the samples (In203-Co0)/Zr02 arc characterized by high moisture and sulfur resistance (NO conversion in SCR by methane reaches 86 % at 300°C al the presence of H2O).
49

NOEA 2011
Zakopane 4-7 September 2011
Tab. 1. Activity of binary Co-ln-oxide catalysts in SCR NO by CH4 /0.05 % NO + 0.09 % CH4 + 5%O2 + (9%H2O;+ 0.01 % SO2) + Ar/; GHSV= 12000 h1
	Catalyst composition	NO Conversion,	% / T, °C of achievement in reaction
	(preparation method) */	mixes
		NO+CH4	NO+CH4+O2+	NO+
		+o2 h2o		CH4+O2+SO2
	2.5%CoO-2.5%In2O1/Al2O1	28/350
(I)
	5%CoO / (5%ln2O3-AI2O3)	37/350
(coprecipitated) (I)
	5%CoO-5%In203/Zr02 (I)	60/350	72/350	45/350
	2.5%In20j -5%CoO/ZrQ2	72/350	75-86/300-350	65/350
(II)

*/1 - impregnation of carriers with: 1) indium salts, 2) cobalt salts;
11 - impregnation of carriers with: I) cobalt salts, 2) indium salts.
Data on activity of Co-oxide catalysts on the various carriers pul on matrixes of honeycomb structure in SCR (N2O+NO) by CHi and C3H8-C4H|O are presented in Tab. 2.
Tab. 2. Activity of structured cobalt-oxide catalysts in reduction of N2O and NO depending on the composition of the secondary carrier (GHSV = 6,000 h'1).
Catalyst	Conversion N2O[NO],%/T,°C (Tso%) for reaction mixes:	Conversion NO, %/T, °C
0,2 % N2O + 0,1% NO + 0,l%C3-C4	0,2 % N2O + 0,1% NO +0,l%C3-C4 + 2,5% O2	0,05 % NO + 0,09%CH4 / +5 % O2
5%CoO/ZrO2	83/400(320)1	78/500(450)1	58/3002
CoO/ZrO2/ kaolin - aerosil	[71/455 (370)]1	[24/350]
72/500 (470)	38/560	53-60/300-370
CoO / (ZrO2-Al203) 1		23/550	46-56 / 300-370
cordierite
CoO / (H-ZSM-5 - A12O3) / cordierite	83/500 (460)	58/560 (545)	50-60/350

'/conversion N2O [NO] for a mix of 0,5 % N2O + 0,25 %NO+0,2%C3-C4 + 5%O2,
^conversion NO for a mix of 0,2 % N2O + 0,1 %NO+0,5%CH4 + 5%O2.
Conversion of N2O at the presence of NO in reduction by propanc-bulane mixture is reached of 72-83 % at 500°C over the samples with different secondary carriers and matrixes of honeycomb structure. In the conditions of SCR conversion of N2O decreases to 38-58 % and is reached at more heats (560°C). Decrease in N2O conversion on the structured catalysts in comparison with the granulated can be connected with some decrease of both specific and active surface of the samples.
Synthesised composites Pd/(Co304-Ce02-(Zr02)/cordierite show high activity in reactions of TWC (CO/NO/C6HI4), in particular in reactions NO(N2O)+CO. They also have shown high activity and sulfur resistance in reaction mixes NO+CO+O2+H2O+SO2 in comparison with the catalyst on the base of Pd-Rh. This is caused by formation of high dispersed (10-30 nm) ordered nanostructures into which Co3O4-CeO2 and Pd enter according to results of XRD, TEM, SEM [3].
50

NOEA2011
Zakopane 4-7 September 2011
[ 1 ] J. Perez-Ramirez, E Kapteijn, K. Schoffel, et al., Appl. Catal. B 44 (2003) 117
1. T. Boichuk, V. Struzhko, S. Oriyk, Russ. J. Appl. Chem. 83 (2010) 1742
2. P. Kirienko, S. Soloviev, S Oriyk, Theor. Experim. Chem. 46 (2010) 39

NOEA201I
Zakopane 4-7 September 2011
P06
##### Strategy of NOx reduction for the Diesel engines of light passenger cars ■J.-M. TRICHARD1
Renault - DREAM/DlMat - Guyancourt, France
The NOx emission reduction will be the main issue for Diesel engine for the next decade. Due to the CO2 emissions reduction requirement, this NOx reduction has to be done without losing the engine Diesel benefit on fuel consumption.
The two after-treatment systems in competition to reduce NOx are the NOxTrap and the Selective Catalytic Reduction with ammonia injection (SCR-NH3), which have different performances and constraints.
After an adsorption period (the system traps the NOx), the NOxTrap requires a regeneration phase (in fact a rich incursion with fuel injections) enabling the reduction of accumulated NOx. The engine combustion strategies carried on imply an increase of fuel diluted in engine lubricant, but also supplementary un-burnt HC emissions. This after-treatment system is poisoned by sulfur (present in fuel and in engine lubricant) and must be recurrently desulfated (these desulfations are more severe than NOxTrap regenerations, rising concerns about the engine reliability, the over-consumption and the emitted HC). In spite of these efforts, a part of sulfur adsorption on the NOxTrap active sites (those normally dedicated to NOx storage) becomes irreversible and a slow process of system poisoning has to be addressed.
The selective catalytic reduction with ammonia is a continuous process for NOx treatment and shows very efficient treatment efficiency. But, this technology needs to add in the vehicle an additional tank for the urea storage. Moreover, this technology is very constrained from an architectural point of view because two catalysts systems may be necessary before and after the DeNOx catalyst: one to hydrolyze the urea and form the ammonia and one to prevent the NH3 release in the exhaust line. We will give a comparison between these two systems. Some perspectives and progress, and cost issues will be discussed.
Nevertheless, Diesel engine makes also progress on pollutants emissions and fuel consumption by the injection system and air loop management improvement.
In its challenge for the preservation of the Environment, the european car manufacturers favor the Diesel, which must comply with the most stringent standards constraints. For the Diesel, the combination of after-treatment and combustion system, in order to reach a good compromise between cost and performance, could be adapted according to the performances and the range side of the vehicles.

NOEA2011
Zakopane 4-7 September 2011
C04
##### Selective Catalytic Reduction of NOx by diesel fuel: plasma-assisted HC/SCR system
##### B. K. CHO2*, J.-H. LEE2, C. C. CRELLIN2, K. OLSON2, D. L. HILDEN2, M. K. KIM1, P. S. KIM1,1. HEO1, L-S. NAM1*
1 Department of Chemical Engineering/School of Environmental Science and Engineering,
Pohang University of Science and Technology (POSTECH),
San 31 Hyoja, Pohang, 790-784, Korea
General Motors Global R&D Center, 30500 Mound Road, Warren,
Ml, 48090-9055, USA
* Tel: +82-54-279-2264, Fax: +82-54-279-8299,
e-mail: bbkcho@postech.ac.kr or isnam@postech.ac.kr
The selective catalytic reduction of NOx by urea (urea/SCR) and the lean NOx trap technology (LNT) are the two most efficient NOx reduction technologies currently available for diesel engine emission control. Both technologies provide good NOx reduction performance over a wide temperature range (200-400°C) under well-controlled conditions, but have serious drawbacks of their own; for example, an additional urea tank to be refilled periodically alongside a urea infrastructure (urea/SCR) and the high cost of noble metals with complex engine control (LNT) [1-3], As a promising alternative without those drawbacks inherent in the urea/SCR and the LNT, the SCR by fuel hydrocarbon (HC/SCR) has been extensively investigated as well [4-7]. However, its low temperature deNOx performance is not yet sufficient for effective commercial implementation. The objective of this collaborative research work is to develop a viable alternative deNOx technology for diesel engine exhausts that can use the onboard diesel fuel as the reductant, without the shortcomings of the urea/SCR and the LNT technologies.
A plasma-assisted NOx reduction system has been developed for diesel engine exhausts, where raw diesel fuel is reformed to produce oxygenated hydrocarbons (OHC) that can be subsequently used for NOx reduction over suitable OHC/SCR catalysts such as BaY, CuY and Ag/Al2O3 catalysts. The system consists of a sidestream hyperplasma reactor (Fig. 1), a diesel fuel reformer and a dual-bed catalytic reactor. A unique feature of this system is a plasma-induced diesel fuel reformer that can produce highly reactive OHC’s for NOx reduction. The steady-state performance as well as the simulated FTP performance for NOx reduction has been evaluated using a combined hyperplasma/fuel reformer/catalyst system installed in a sidestream connected to the main exhaust stream of a 4.9L, 6-cylinder Isuzu diesel engine dynamometer system. For comparative kinetic studies, laboratory microreactor experiments have also been conducted for the OHC/SCR using ethanol, E-diesel or a mixture of simulated diesel fuel and ethanol as the reductant.
The NOx reduction potential of the system has been successfully demonstrated through both steady­state and simulated FTP tests using an engine dynamometer system. Results of these tests have clearly demonstrated the beneficial effect of the OHCs as NOx reductants at low temperatures. The reformed diesel fuel has proven to be as effective as E-diesel as the reductant for NOx reduction above 225°C. The beneficial effect of the in-situ generated OHCs is compared with that of ethanol and E-diesel in both laboratory microreaclor experiments and engine dynamometer tests. The enhanced deNOx activity of the hybrid system developed in this work is compared with that of the NH^SCR, the industry benchmark deNOx technology. Included also in the discussion is the fuel economy penalty associated with both the external fuel injection for the NOx reduction and the plasma power consumption for the fuel reformer. Finally, reaction mechanisms will be proposed to explain both the role of plasma in the fuel reformer and the enhanced activity of the HC/SCR catalyst due to the presence of OHCs in the feed stream.
55

NOEA 2011
Zakopane 4-7 September 2011
Figure I. Hyperplasma reactor
Time
Figure 2. Effect of plasma on NOx concentration
Listed below are the major findings of this work.
1. The enhanced deNOx performance of a plasma-assisted HC/SCR system for diesel engine exhaust has been validated in a series of engine dynamometer tests (Fig. 2). The OHCs from the reformed diesel fuel has proven to be as effective as E-diesel for NOx reduction, except at low temperatures below 250°C.
2. Both (BaY+CuY) and (BaY+Ag/Al2O3) dual-bed catalysts work well for the NOx reduction in this OHC/SCR system. A mode-average NOx conversion of 61% has been achieved during simulated FTP tests with the (BaY+CuY) dual-bed catalyst.
3. The C,/NOx feed ratio to the catalyst has been identified as one of the most critical operating parameters affecting the NOx conversion. For example, NOx conversions of 60% and 99% have been
56

NOEA20I1
Zakopane 4-7 September 2011
obtained for the C|/NOx feed ratios of 6.5 and 20, respectively at 325°C over the (BaY+Ag/AI2O3) dual-bed catalyst.
1. The fuel economy penalty of the system has been estimated to be 3.9%, including both external fuel injection and plasma power supply.
2. With further improvement, the plasma-assisted HC/SCR can be a promising alternative to the urea/SCR and ENT technologies.
[ 1 ] J. H. Baik, S. D. Yim, I.-S. Nam, Ind, Eng. Chem. Res. 45 (2006) 5258
1. P. Forzatti, I. Nova, E. Tronconi, Angew. Chem. Int. Ed. 48 (2009) 8366
2. C. H. Kim, G. Qi, K. Dahlberg, W. Li, Science 327 (2010) 1624
3. R. Burch, J. P. Breen, F.C. Meunier, Appl. Catal. B 39 (2002) 283
4. S. J. Schmieg, B. K. Cho, S. H. Oh, Appl. Catal. B 49 (2004) 113
5. B. Wen, Y. H. Yeom, E Weitz, W. M. H. Sachtler, Appl. Catal. B 48 (2004) 125
6. M. K. Kim, P. S. Kim, J. H. Baik, I.-S. Nam, B. K. Cho, S. H. Oh, Appl. Catal. B 105 (2011) 1

NOEA2011
Zakopane 4-7 September 2011
Kil
##### Catalytic behavior of combined LNT/SCR systems
##### P. FORZATTI1, L. LIETTI1, L. CASTOLDI1, R. BONZI1, S. MORANDI2, G. GHIOTTI2, S. DŹWIGAJ3
1 Dipartimento di Energia, LCCP, Politecnico di Milano,
P.zas L. da Vinci, 32 - Milano, Italy
2 Dipartimento di Chimica 1FM and NIS, Universita di Torino,
Via P. Giuria, 7 - Torino, Italy
1. CNRS, UMR 7197, Laboratoire de Reactivite de Surface, Universite Pierre et Marie Curie,
2. place Jussieu, Paris Cedex 05, France
While compliance with previous regulations of NOX emission under lean conditions in vehicles has been achieved without resort to NOX after-treatment, either Nitrogen Storage Reduction or Selective Catalytic Reduction will be needed in the future to meet the upcoming more stringent NOX emission standards. A third approach to lean NOX control is the use of hybrid LNT+SCR systems [1,2,3,4].
In this work the NOX storage-reduction over the single Pt-Ba/Al2O3 and Fe-ZSM-5 systems and over the hybrid Pt-Ba/Al2O3 + Fe-ZSM-5 systems, both physically mixed and in dual bed configuration with the SCR catalyst placed downstream of the LNT catalyst, is systematically investigated by ISC (Isothermal Step Concentration) experiments and combined FTIR spectroscopy. The study is accomplished using H2 as the reductant, in the presence and absence of CO2 and H2O and in a wide temperature interval (150-350°C) [5],
The storage of NOX starting from NO/O2 occurs via the nitrite route which implies a stepwise oxidation of NO to give nitrite ad-species followed by oxidation of these species to give nitrates. The reduction of stored NOX occurs through a 2 steps consecutive scheme, which implies at first the reduction of nitrates by H2 to give NH3, followed by the reaction of ammonia with NOX stored downstream in the reactor to give N2.
The following main points have been clarified at the qualitative-quantitative level: 1) the storage of NOX occurs primarily onto Pt-Ba/Al2O3 and is lower in the presence of CO2 and H2O because BaCO3 is formed which retards NOX adsorption; 2) NH3 formed as intermediate in the reduction of stored NOX is trapped onto the Fe-ZSM-5 catalyst. The trapping of NH3 is most favoured when the particles of Pt-Ba/AI2O3 and of Fe-ZSM-5 are extensively in intimate contact, as in the LNT/SCR physical mixture, and at low temperature. NH3 trapped onto Fe-ZSM-5 reacts during the subsequent lean phase with gaseous NOX slipped from the Pt-Ba/Al2O3 particles to give N2 via SCR; 3) the NOX removal efficiency is always higher for both LNT/SCR dual bed and physical mixture compared to single LNT, due to the additional contribution of SCR over Fe-ZSM-5 during the lean phase; 4) in the case of the LNT/SCR physical mixture, NH3 trapped onto the Fe-ZSM-5 particles can be oxidized over the LNT particles upon admission of oxygen to give N2, N2O and NO. The selectivity to nitrogen is almost complete at any temperature in the presence of CO2 and H2O while in the absence of CO2 and H2O it increases significantly with temperature and is almost complete at 350°C; 5) the ammonia slip is low to the best over the LNT/SCR dual bed at any temperature in the absence of CO2 + H2O. In the presence of CO2 and H2O the ammonia slip is nil at any temperature over the LNT/SCR dual bed.
[ 1 ] T. Johnson, Platinum Metals Rev. 52 (2008) 23
1. P. Forzatli, Appl. Caul. A 222 (2001) 221
2. N. Takahashi, H. Shinjoh, T. Iijima, T. Suzuki, K. Yamazaki, K. YokoU, H. Suzuki, N. Niyoshi, S. Matsumoto, S. Tanizawa, S. Tanaka, T. Tateishi, K. Kashara, Caul. Today 27 (1996) 63
3. M. Weibel, N. WaldbiiBer, R. Wunsch, D. Chatterjee, B. Bandl-Konrad, B. Krutzsch, Top. Caul. 52 (2009) 1702
59

NOEA2011
Zakopane 4-7 September 2011
[5] L. Castoldi, R. Bonzi, L. Lietti, P. Forzatti, S. Morandi, G. Ghiotli, S. Dźwigaj, J. Calal. 2011, in press

NOEA2011
Zakopane 4-7 September 2011
C05
#### Effect of thermal aging on surface morphology and performances of commercial Lean NOX Traps
#### D. ADOUANE1, P. Da COSTA1, P. DARCY2
1 Universite Pierre et Marie Curie (Paris VI), Institut Jean le Rond d’ALAMBERT,
CNRS UMR 7180, 2 Place de la Care de Ceinture 78210 Saint Cyr I’Ecole, France,
e-mail: dihya. adouane @ upmc.fr
2 Technocentre Renault, I avenue du Golf 78288 Guyancourt Cedex
In recent years, great efforts have been shown by car manufacturers in order to reduce the ecological impact of their vehicles by developing different technologies to limit emission of such air pollutants. One of the most efficient technologies is the lean NOx traps (LNT) [ 1], LNTs are formulated with a storage component, usually alkali or alkaline earth metals, such as barium or potassium, and precious metals over a high surface area y-Al2O3 support [2-3-4]. During lean operation, NOx are trapped on the storage component in the form of nitrates. For short periods the engine is operated slightly rich such that the stored nitrates are released as NOx and subsequently reduced to N2 by CO and H2. The catalyst deactivation is mainly due to sulfur poisoning and thermal aging [5]. To meet the durability requirement of DeNOx catalysts, an improved understanding of the impact of thermal aging on catalyst structure and activity is needed. This paper presents the results from a study on the effects of thermal aging on the lean NOx Trap structure and activity.
The LNT formulation used in the laboratory study was similar to the LNT used on the first cars equipped with a NOx-Trap. A 400 cpsi, fully-formulated LNT catalyst sample with a diameter of 27 mm and a length of 50 mm is placed in a quartz tube. The reactor is a 370 mm long quartz tube with a 30 mm outside diameter placed inside an oven. Type-K thermocouple is used to measure the axial temperature variation across the LNT. Samples were aged under gaseous mixture of 90% air and 10% of water for 5 hours at temperatures of 750°C and 800°C. The fresh and aging catalysts were characterized by XRD, XPS, SEM and TEM microscopy and their catalytic performances were studied on a synthetic bench gaz.
Figure I. Transmission Electron Microscopy results (TEM)- (a): Fresh NOx-Trap- (b)-aging NOx-Trap 5h750°C- aging NOx-Trap 5h800°C- (1): Platinum particles sintering- (2): barium carbonates particles sintering
61

NOEA 2011
Zakopane 4-7 September 2011
The first resulLs show that exposure to high temperatures causes the sintering of platinum particles from 7nm on the fresh LNT to 22nm, which leads to reduce the ability of the LNT to oxidize NO to NO2. Similarly, high temperatures cause the loss of surface area of storage materials, reducing the number of storage sites and therefore the NOx storage capacity. Barium carbonates particles sintering and migration were also observed after thermal aging.
1. N. Takahashi, H. Shinjoh, T. Iijima, T. Suzuki, K. Yamazaki, K. Yokota, H. Suzuki, N. Miyoshi, S. Matsumoto, T. Tanizawa, T.Tanaka, S. Tateishi, K. Kasahara, Catal.Today 27 (1996) 63
2. Hiroki Hosoe, Masahiro Sakanushi, Kimihiro Tokushima, Tadao Nishiyama, Shogo Konya, Masyuki Kasuya, Masato Kaneeda, Hidehiro Lizuka, SAE Technical papers 2008-01-0806
3. Kinichi Iwachido, Takayuki Onodera, Tetsuya Watanabe, Mariko Koyama, Akihisa Okumura, Masao Hori, SAE Technical Papers 2009-01-1077
4. Sounak Roy, Alfons Baiker, Chem Rev, 2009,109,4054
5. P.N. Le, E. C. Corbos, X. Courtois, F. Can, S. Royer, P. Marecot, D. Duprez, Top.Catal. (2009) 52:1771

NOEA2011
Zakopane 4-7 September 2011
C06
##### Modelling of N2O formation during the regeneration of NOX storage catalyst
##### Ś. BARTOVA1, P. KOCI*', M. MAREK1, J. PIHL2, J.-S. CHOI2, W. PARTRIDGE2
1 Institute of Chemical Technology, Prague, Department of Chemical Engineering,
Technicka 5, CZ-166 28 Prague, Czech Republic
1 Oak Ridge National Laboratory, Fuels, Engines & Emissions Research Center,
2360 Cherahala Blvd., TN-379 32 Knoxville, USA
^Corresponding author, Email: petr.koci@vscht.cz, http://www.vscht.cz/monolith
Periodically operated NOX storage and reduction catalyst (NSRC, NOX adsorber, or lean NOX trap, LNT) is one of the available catalytic technologies used for abatement of NOX emissions from lean-bum engines (both gasoline and Diesel). Reducing front moves along the catalytic monolith channel during the NSRC regeneration, dividing the catalyst into two parts - the front one is already reduced while the rear one is yet in an oxidized state with a high surface coverage of the stored oxygen and NOX. Gas transport along the catalytic channel then enables multiple transformations of nitrogen compounds.
Recently, a spatially distributed LNT model with global kinetics has been developed that describes NOX storage, formation of N2 and NH3 during the regeneration and subsequent ammonia re-oxidation in the yet oxidized part of the monolith. The model is able to predict NOX conversions, delay of the outlet ammonia peak after the start of the regeneration, and integral NH3 selectivities in a wide range of operating conditions, incl. real driving cycles [I].
In this contribution we focus on the N2O formation during the LNT regeneration. It can be assumed that the main N2O source is the NH3 re-oxidation - ammonia is the major product in the reduced front part of the monolith, and the formed NH} is then transported into the rear part of the monolith with high oxygen and NOX coverage. To verify this assumption, the NH3+O2 and NH3+NO reactions are investigated both in steady state [2] and transient experiments.
Depending on temperature, the steady-state NH3+O2 reaction leads to three products: N2, N2O and NO. The maximum N2O production is observed at intermediate temperatures, while the NO is the major product at high temperatures (cf. Fig. la). Interestingly, the NH3 conversion and N2O selectivity do not depend much on the NH3:O2 ratio. However, practically no N2O is detected in transient reaction of NH3 with the pre-stored oxygen.
For the second studied reaction (NH3+NO), the steady-state N2O formation curve exhibits similar trend with a maximum, but it is shifted to somewhat lower temperatures (cf. Fig. lb). The N2O is formed accordingly also in transient reaction of NH3 with pre-stored NOX.
63

NOE A 2011
Zakopane 4-7 September 2011
a)
b)
Figure I. a) Temperature dependence of the N2O formation during steady-state NH3+O2 reaction, b) Temperature dependence of the N2O formation during steady-state NH3+NOX reaction.
Based on these experimental results, the NH3 oxidation selectivities towards N2O and NO are evaluated in dependence on temperature and implemented into the existing mathematical model. After the above-described extension of the LNT model, both long and short lean/rich cycles were measured and simulated (cf. Fig. 2, 3).
64

NOEA2011
Zakopane 4-7 September 2011
Figure 2. Experimentally observed and simulated evolution of the outlet NOx, N2O and NH} concentrations during 900 s/600 s long lean/rich cycling performed at a) 200 °C and b) 400 °C. The lean/rich inlet gas composition: 300/0 ppm NO, 0/625 ppm CO, 0/375 ppm H2, 10/0 % O2, always 5 % H2O, 5 % CO2, N2 balance.
65

NOE A 2011
Zakopane 4-7 September 2011
Figure 3. Experimentally observed and simulated evolution of the outlet N0x, N20 and NH3 concentrations during 60 s/5 s short lean/rich cycling at a) 200 °C and b) 500 °C (note: scale change for NH3 and N2O - decreasing magnitude). The ilean/rich nlet gas composition: 300/0 ppm NO, 0/3.4 % H2, 10/0 % O2, always 5 % H2O, 5 % CO2, N2 balance.
The results reveal that the used assumptions are acceptable and the model gives a reasonable prediction of the N2O formation (in terms of both dynamics and magnitude of the N2O peaks) in a wide range of operating conditions.
1. P. Koćf, F. Plat, J. Śtepanek, Ś. Bartova, M. Marek, M. Kubićek, V. SchmeiBer, D. Chatterjee, M. Weibel, Catal. Today 147S (2009) S257
2. J. A. Pihl, J. E. Parks II, C. S. Daw, T. W. Root, SAE Tech. Paper 2006-01-3441 (2006)
66

NOEA20I1
Zakopane 4-7 September 2011
C07
##### NO reduction by H2 on Rh-based catalyst for Natural Gas vehicles: Study of active sites by operando IR spectroscopy
##### S. CARRE1, Y. RENEME1, F. DHAINAUT1, C. DUJARDIN1, P. GRANGER1
1 Universite Lille Nord de France, UCCS,
CNRS UMR818I, 59650 Villeneuve d’Ascq, France, e-mail: sonia.carre@univ-lilleI,fr
Research and development of alternative fuels for passenger cars and heavy duty vehicles are of great importance to solve various environmental problems associated with atmospheric pollutant emissions from combustion engines. Natural gas can be profitably used as alternative fuel and offers a good compromise between efficiency, due to homogeneous combustion, and low atmospheric pollutant emissions, such as CO. However, some drawbacks still remain associated with NOX and CH4 emissions that must be controlled. Three-way catalysts for gasoline engine are not always adapted for Natural Gas Vehicles (NGV), in fact methane combustion requires high residual temperature, and are sensitive to deactivation. Consequently, the development of catalysts containing lower amounts of noble metal and being more resistant to thermal sintering is a challenging task.
This work compares classical kinetic approach and operando experiments of NO/H2/O2 reaction under various operative conditions on model Rh-based catalysts.
Rh(0.18wt%)/AI2O3 and Rh(0.18%)/Ceo.7Zr0302/Al203 catalysts were prepared according to a conventional wet impregnation method using nitrate precursor in aqueous solution [I]. Classical temperature-programmed and steady-slate rate experiments were performed in an optimised Infrared reactor cell (Diffuse Reflectance IR cell) with gas hour space velocity fixed to 10000 h1. IR spectra of adsorbed species were recorded in temperature programmed conditions or steady-state conditions. At the same lime, products (NO, NO2, H2, O2, N2, NH3, N2O) were quantified with a gas chromatograph Varian CP490 and a FTIR spectrometer (Thermo 480) equipped with a IR cell for gas analysis.
Previous kinetic study suggest that two reaction mechanisms for the dissociation of NO can coexist on Pd/Al2O3 catalyst and utilize either a free site (eq. I), or an adsorbed hydrogen atom (eq. 2); the decomposition implying a free site does not seem negligible. On the other hand on the Rh/Al2O3 catalyst, only the dissociation assisted by adsorbed hydrogen was highlighted.
NOjjs + <-» Nads + Oajs eq. 1
NOads + Hads <-> Nads + OHjds eq. 2
Temperalure-programmed reaction was performed in stoichiometric conditions in order to promote the NO reduction to N2 in parallel to H2 oxidation to H2O (Figure 1). NO is activated on Rh/Al2O3 catalyst above 100°C and leads to the formation of nitrous oxide and nitrogen below 250°C. Above 250°C, the formation of ammonia and nitrogen predominates. On Rh/CeZrO2-Al2O3 (Figure 2), total conversion of NO is achieved above 180°C. Changes in selectivity occur. At low temperature (<150°C) N2O and N2 formation is observed, N2 remains predominant. Above I5O°C, ammonia is produced, but in lower extent than in the case of Rh/Al2O3. The nitrogen yield reaches 100% at higher temperature. Clearly, the deposition of rhodium on ceria-zirconia improves catalytic properties on NO reduction with higher selectivity to nitrogen.
67

NOEA2011
Zakopane 4-7 September 2011
Figure I: Temperature-programmed reaction under 950ppm NO, 3000ppm H2, 1025ppm O2 after stabilization in IR cell on pre-reduced Rh/Al2O3
Figure 2: Temperature-programmed reaction under 950ppm NO, 3000ppm H2, 1025ppm O2 after stabilization in IR cell on calcined Rh/Ceo,2Zr0302-Al203
At the same time, surface adsorbed species are recorded and mainly consist on nitrosyl, nitrite and nitrate species. On Rh/Al2O3 at 20°C, three main bands of nitrosyIs were found: RhfNO)6* around 1896 cm’1, Rh(NO)° at 1820 cm’1 and RhfNO)6- around 1714 cm1. With the increase of the reaction temperature to 130°C, the disappearance of Rh(NO)° and Rh(NO)8" at the expanse of Rh(NO)^ is observed. At higher temperature (>200°C), no nitrosyls were present at the surface, in agreement with the total conversion of NO in this range. The formation of RhfNO)4* at 1905 cm’1 is also detected between 25 and 100°C on freshly calcined Rh/CeZrO2-Al2O3 catalyst in the presence of 950ppm NO, 3000ppm H2,1025ppm O2.
The nature of nitrosyls absorbed species on Rh may influence the reactivity suggested by elementary steps from mechanism. The reactivity of nitrosyls species was also examined using transient experiments at low temperature. Relations between catalytic performances and spectroscopic measurements will be discussed in the presentation.
[1] Y. Rename, F. Dhainaut, M. Frere, B. Ravanbakhsh, P. Granger, C. Dujardin, P.L. De Cola, Surf. Interface Anal. 42 530 (2010)
68

NOE A 2011
Zakopane 4-7 September 2011
C08
##### Controlling the surface dispersion of bao nano-domains on catalytic NOX storage materials via TiC>2 anchoring sites and improvement of sulfur poisoning tolerance
##### E. ÓZENSOY1*, G. SEDA VENTURE1, E. VOVK1
1 Department of Chemistry, Bilkent University, Ankara 06800, Turkey
^Corresponding author: ozensoy@fen.bilkent.edu.tr
TiO2 promoted novel NO, storage materials were synthesized in the form of BaO/TiO2/Al2O3. The structure and the catalytic performance of these novel materials were investigated via TEM, SEM, EDX, Raman, BET, XRD, in-situ FTIR and TPD. Our results indicate that TiO2 nano-domains can be effectively exploited to control the surface dispersion of BaO at the nanoscale and improve the sulfur poisoning tolerance of the NSR catalysts.
Sulfur poisoning is a frequently observed catalytic deactivation phenomenon in heterogeneous catalysis. As a result, accumulation of SOX species in the form of sulfates, sulfites or sulfides on metal and/or metal oxide surfaces have been thoroughly studied in the literature in relevance to three-way catalysis (TWC), selective catalytic reduction (SCR), NOX storage reduction (NSR), hydrodesulfurization (HDS) and Claus process, in which various forms of A12O3 are commonly utilized as the catalytic support material. Two major deactivation phenomena are often reported for the NSR catalysts where A12O3 is used as a conventional support material. The first deactivation route involves thermal degradation of the structural integrity of the catalyst material due to solid state reactions between the catalytic components and sintering while the second one is associated with the sulfur poisoning. In our previous studies [1-3], we have investigated the effect of TiO2 and FeOx on the surface distribution and the thermal stability of the NOX species formed during the nitration of the promoted support materials (TiOx/Al2O3 and FeO,/Al2O3) as well as promoted NOX storage materials (BaO/TiOx/Al2O3 and BaO/FeOx/AI2O3). In the current work [4], we focus our attention on the interaction of SOX with the TiO2/Al2O3 and BaO/TiO2/Al2O3 surfaces as well as the influence of TiO2 domains on the NOX uptake after deactivation by SO2 (g) + O2 (g).
Titania is used as a promoter to obtain novel catalytic support materials in the form of TiO2/Al2O3 (Ti/AI) for NOX storage reduction (NSR) applications. Two different sol-gel preparation protocols (Pl, P2) were utilized in the synthesis, to obtain Ti/AI materials with different surface structures and morphologies at the nano-scale. Ti/Al(Pl) manifests itself as small (-10 nm) crystallites of TiO2 (anatase) on y-AI2O3, while Ti/Al(P2)reveals an amorphous Al,TiyOz mixed oxide. The synthesized NOX storage materials were studied via XRD, Raman spectroscopy, BET surface area analysis, TPD, XPS, SEM, EDX-mapping and in-situ FTIR spectroscopy of adsorbed NO2.
NOX uptake properties of the BaO/TiO2/y-Al2O3 materials were found to be strongly influenced by the morphology and the surface structure of the TiO2/TiOx domains. The presence of Ti4+ surface sites provide additional NO, adsorption sites which can store NO, predominantly in the form of bridged/bidenlate nitrates. An improved Ba surface dispersion was observed for the BaO/TiO2/y-AI2O3 materials synthesized via the co-precipitation of alkoxide precursors which was found to originate mostly from the increased fraction of accessible TiO2/TiOx sites on the surface. These TiO2/TiOx sites function as strong anchoring sites for surface BaO domains and can be tailored to enhance surface dispersion of BaO.
TPD experiments suggested the presence of at least two different types of NO, species adsorbed on the TiO2/TiO, sites, with distinctively different thermal stabilities. The relative stability of the NO, species adsorbed on the BaO/TiO2/y-AI2O3 system was found to increase in the following order: NO7N2O3 on alumina « nitrates on alumina < surface nitrates on BaO < bridged/bidentate nitrates on large/isolated TiO2 clusters < bulk nitrates on BaO on alumina surface and bridged/bidentate nitrates on small TiO2 crystallites homogenously distributed on the surface < bulk nitrates on the BaO sites located on the TiO2 domains.
69

NOEA2011
Zakopane 4-7 September 2011
The functionality/performance of these materials upon SO, and subsequent NO, adsorption were investigated with temperature programmed desorption (TPD) and in-situ Fourier transform infrared (FTTR) spectroscopy.
Figure 1. (a-d) FTIR spectra obtained after the saturation of fresh (black curves) and sulphur- poisoned (red curves) y-Al2O3, TiO2 (anatase), Fi/Al (Pl) and Ti/Al (P2) surfaces with NO2 at room temperature, respectively.
SO, adsorbs much stronger on pure y-Al2O3 with respect to pure TiQ: (anatase). Nitration of the Ti/Al (P1,P2) support materials poisoned with SO, led to a decrease in the total NO, uptake and lowered the NO, adsorption strength. Overall stabilities of the adsorbed SO, species tend to increase in the following order: TiO2 (anatase)« y-Al2O3 < Ti/Al (Pl) = Ti/Al (P2). Our results reveal that promotion of the conventional y-AI2O3 support material with TiO2 in the form of Ti/Al (P1,P2) leads to a larger SO, uptake. Thus, unlike the acidic TiO2 (anatase) surface, which has a relatively limited SO, uptake with respect to y-Al2O3, synthesized Ti/Al (P1.P2) mixed oxides reveal new additional SO, storage sites. These sites may function as sacrificial SO, binding sites in NSR catalysts by preventing the sulfur poisoning of the alkali or alkaline earth oxide sites used as NO, storage units.
E. Kayhan, S. M. Andonova, G. S. Senturk, C. C. Chusuei, E. Ozensoy, J. Phys. Chem. C 114 (2010)357
70

NOEA20I1
Zakopane 4-7 September 2011
C09
##### NOx reduction and methane oxidation over mesoporous silica supported palladium
##### J. BASSIL1, A. A1BARAZI2, P. Da COSTA2, M. BOUTROS1
1 Universite Libanaise, Faculte des sciences II,
Laboratoire de Chimie Physique des Materiaux (LCPM), Campus Fanar,
BP 90656, Jdeideh - Liban, e-mail: boutrosmaya@hotmail.com
2 Universite Pierre et Marie Curie, UPMC Paris 6,
Institut Jean Le rond d'Alembert (UMR 7910), 2 place de la gare de ceinture,
78210 Saint Cyr I’ecole, France, patrick.da_costa@upmc.fr
Silica or aluminosilica with an hexagonal structured mesopore network like MCM-41 and SBA-15 are characterized by high specific surface area, porous volume and adjustable pore size diameter make them ideal support of catalysts. Such mesoporous silica SBA-15, modified with copper, iron, Mn, were already studied in SCR of NO by ammonia [ 1 ]. This technology is not so easy to implement on automotive field due to difficulties in the storing or handling of NH3. The abundance of methane makes the SCR of NO, by methane a promising and attractive technology for the abatement of NO, emissions from stationary sources [2]. In this work, some materials Pd-SBA-15 were synthesized and characterized by various techniques.We investigate the influence of the impregnation method on the physico-chemical properties of SBA-15 support, the morphology of palladium nanoparticles and the catalytic performances of mesoporous supported palladium catalysts in methane oxidation and NO, reduction by CH4.
The mesoporous silica SBA-15 was synthesized using a hydrothermal method described by Zhao et al [3], The palladium precursor used is tetramine palladium(II) nitrate Pd(NH3)4(NO3)2. The catalysts Pd-SBA-15 were prepared by ion exchange method (Pd-SBA-15(IE)) or incipient wetness impregnation (Pd-SBA-15(IWI)). Then, the samples were calcined under air flow at 500°C for 2 h.
The catalysts were characterized by various techniques and tested for the reduction of NO, by methane in the presence of oxygen (500 ppm NO + 1500 ppm CH4 + 7% O2 in Ar; GHSV = 22100 h1).
The structure and the mesoporosity of the different solids were determined by their low-angle XRD patterns and N2 sorption isotherms, respectively.
Compared to the pure calcined silica SBA-15, Figure 1 shows that Pd-SBA-15 (IWI) has three well-resolved characteristic diffraction peaks which are attributed to 100, 110 and 200 of hexagonal structure. In the case of Pd-SBA-15 (IE), (Fig. I curve c), a gradual decrease of the intensities of each peak is observed, related to the strongly alcaline medium used during the method of impregnation.
Il was noticed that the diffraction peaks of palladium containing mesoporous silica, are less shifted to higher values than those of pure SBA-15 silica related to a decrease of structural parameters (dhkl and ao). This difference is maybe related to the presence of Pd particles inside the mesopores channels of SBA-15 support.
N2 adsorption-desorption isotherms of calcined SBA-15 support and Pd-SBA-15 samples exhibit characteristic type IV isotherms with a Hl hysteresis loop as defined by IUPAC (Figures not shown). The textural parameters of the Pd-SBA-15 samples prepared with two different methods of impregnation are listed in Table 1. The inclusion of palladium by ion exchange into the structure of SBA-15 conducted to a large modification of the specific surface area (- 35%) that is not the case of Pd-SBA-15 (IWI) sample (- 17%).
71

NOE A 2011
Zakopane 4-7 September 2011
Table I: Physico-chemical properties of SB A-15 and Pd-SBA-15 samples
Samples	Si / (wt%)	Pd (wt%)	^BET / (m2 g1)	v / * pores / (cm’g1)	Spores / (nm)
Si-SBA-15	-	-	800	1.15	6.7
Pd-SBA-15 (IWI)	48	0.18	665	0.85	5.5
Pd-SBA-15 (IE)	48	0.25	525	0.75	5.2

TEM images of Pd-SBA-15 samples indicate that these solids are well mesostrutured despite the introduction of metal on the support. Dispersed palladium nanoparticles are mainly located inside the pore channels in the case of Pd-SBA-15 (IE). However, the detection of palladium particles is more difficult for Pd-SBA-15 (IWI) sample.
Small PdO nanoparticles and Pd(II)O clusters species were detected by UV-vis and XRD high angles.
Figure I. X-ray diffraction patterns of (a) SBA-15, (b) Pd-SBA-15 (IWI) and (c) Pd-SBA-15 (IE)
72

NOEA 2011
Zakopane 4-7 September 2011
Temperature (°C)
Figure 2. Steady-state methane conversion as junction of temperature for SBA-15 and Pd-SBA-15 samples
The palladium catalysts prepared on the mesoporous silica have a lower activity for the reduction of NOX by CH4 ( < 10%). The methane oxidation started at about 300°C; then the conversion into CO and CO2 increased drastically with the reaction temperature and the complete conversion was reached al 400°C and 500°C for Pd-SBA-15 (IE) and Pd-SBA-15 (IWI) respectively (Fig. 2).
To conclude, new catalysts were synthesized by depositing Pd on SBA-15. Whatever the method of impregnation, the particles of palladium are very small and well dispersed on the surface of support. The Pd/mesoporous materials demonstrate the better oxidation of methane into CO and CO2.
[ I ] X. Liang,, J. Li,, Q. Lin, K. Sun, Catal. Commun. 8 (2007) 1901
1. R. Marques, L. Mazri, S. Da Costa, F. Delacroix, G. Djega-Mariadassou, P. Da Costa, Catal. Today 137 (2008) 179
2. D. Zhao, Q. Huo, J. Feng, F. Chmelka, G.D. Stucky, J. Am. Chem.Soc. 120 (1998) 6024
73

NOEA 2011
Zakopane 4-7 September 2011
K12
##### Design of the Catalysts for the Removal of Diesel Soot and NOX
##### Z. ZHAO1
1 State Key Laboratory of Heavy Oil Processing, China University of Petroleum,
Beijing 102249, China, e-mail: zhenzhao@cup.edu.cn
Particulate materials (PM, mainly containing diesel soot) and NOx are very serious and most difficult to be removed pollutants emitted from diesel enginefl-5]. The combination of traps and oxidation catalysts appears to be one of the most efficient after-treatment techniques for the removal of diesel PM, and research and development of highly active catalysts for diesel soot combustion become an urgent task. Moreover, the simultaneously catalytic removal of diesel soot particle and NOx is also a very significant method because it can purify the two kinds of serious pollutants from diesel engine exhausts at same time [1,2], In this lecture I will mainly discuss the catalysis nature and the design of the catalysts for the combustion of diesel soot.
On the one hand, the good redox property and the strong ability to activate oxygen of catalysts play significant roles in obtaining high catalytic activity for soot oxidation. Thus, the intrinsic factors including the compositions, structures, the oxidation states, the oxygen vacancy, and the size of catalysts particles are important for the catalysts to getting the high catalytic activity for soot oxidation.
On the other hand, since the soot oxidation over a catalyst is a complicated gas-solid (soot)-solid (catalyst) multiphase reaction, besides the intrinsic factors, the external factors, especially the contact efficiency between catalyst and soot, also plays a significantly important role in the oxidation of soot particles. Based on the literature [1-8] and our group’s recent works [9-19], four ways to promote the contact efficiency between diesel soot particle and catalyst were proposed / summarized. Firstly, the mobility of the ions in the catalysts under the melting conditions is much higher than that under normal solid conditions. The high mobility of the ions in the catalysts is favorable for getting the good contact between catalysts and diesel soot. Therefore, the compounds with low melting points or the two kinds of mixed oxides with low eutectic melting point should be good candidate catalysts for soot oxidation[3,9]. Secondly, nanometric catalysts have high specific surface area and good mobility, which facilitates the contact between diesel soot and catalyst, and decreases the activation energy for diesel soot combustion reaction. Thus it results in the increase of catalytic activities [10-13], Thirdly, the pore diameter of macroporous catalysts is big enough to permit soot particulate to enter their inner pores. And the open pore structure can facilitate the diffusion of soot into the inner pore channel, which offers the advantage of highly accessible surfaces [8,14-18]. Therefore, the contact efficiency is dramatically enhanced. Fourthly, the contact mode among catalyst, diesel soot and reactant gas become into solid-gas-solid contact from solid-solid-gas with the incorporation of strong oxidant, such as NO2 molecule. Therefore, the contact between soot and catalyst can be improved dramatically [3,6,11,19],
The most important character for the highly active catalysts for the combustion of diesel soot is the strong ability to activate oxygen al low reaction temperatures, especially for getting the very low ignition temperature for soot oxidation, which is the most important characteristics that the excellent soot oxidation catalysts should possesses.
In this talk, several systems of the catalysts including the oxides with low melting points, the nano­sized multi-component bulk Co-based, or Mn-based perovskite-type complex oxides, nanometric CeO2-supported cobalt oxides, nano-macroporous Ce-Zr solid solution oxides, nano-macroporous Fe-based, Co-based, or Mn-based perovskite-type complex oxides, and nano-macroporous perovskite LaFeO3-or nano-macroporous Ce-Zr solid solution oxide-supported gold catalysts were summarized and their catalytic performances for diesel soot oxidation were also investigated and compared. The catalysts were characterized by the techniques of N2-adsorption and desorption, SEM.TEM, TG-DTA, XRD, IR, UV-Vis, H2-TPR, O2-TPD and NO-TPD. Moreover, the reaction mechanism of diesel soot oxidation
75

NOEA2011
Zakopane 4-7 September 2011
on the multi-component oxide catalysts was studied by the means of in-situ UV-Raman and MS-TPSR [19].
This work was supported by the National Natural Science Foundation of China (No. 20833011, 20803093 and 21073235), the 863 program of China (No. 2009AA06Z313).
[ 1 ] K. Yoshida, S. Makino, S. Sumiya, G. Muramatsu, et al., SAE Paper 892046 (1989)
1. Y. Teraoka, K. Nakano, S. Kagawa, W.F. Shangguan, Appl. Catal. B 5 (1995) L18
2. J.P.A. Neeft, W. Schipper, G. Mui, et al., Appl. Catal. B 11 (1997) 365
3. N.Russo, S. Furfori, D. Fino, et al., Appl. Catal. B 83 (2008) 85
4. M.Adamowska.A. Krzton, M. Najbar, et al., Appl. Catal. B 90 (2009) 535
5. J. O. Uchisawa, A. Obuchi, Z. Zhao and S. Kushiyama, Appl. Catal. B 18 (1998) LI83
6. A.L. Kustov, M. Makkee, Appl. Catal. B 88 (2009) 263
7. M. Sadakane, T. Asanuma, J. Kubo, et al., Chem. Mater. 17 (2005) 3546
8. J. Liu, Z. Zhao, C. Xu ,el al., Applied Catal. B 61 (2005) 36
9. H. Wang , Z. Zhao, C. Xu, et al., Catal. Letters 102 (2005) 251; 124 (2008) 91
10. J. Liu, Z. Zhao, C. Xu, et al., Applied Catal. B 78 (2008) 61
11. J. Liu, Z. Zhao, C. Xu, et al., Applied Catal. B 84 (2008) 185
12. J. Liu, Z. Zhao, C. Xu, et al., J. Phys Chem. C 113(2009) 17114
13. G. Zhen, Z. Zhao, et al., Chem. Commun. 46 (2010) 457
[ 15] J. Xu, J. Liu, Z. Zhao, et al., I., J. Catal., DOI: 10.1016/j.jcat.2011.03.024 (2011)
[16] J. Xu, J. Liu, Z. Zhao, et al., Catal. Today 153 (2010) 136
[ 17] Y. Wei, J. Liu, Z. Zhao, et al.,, Angew. Chem. Int. Ed 50 (2011) 2326
[18] Y. Wei, J. Liu, Z. Zhao, et al., Energy & Environ. Sci, DOI:l0.1039/C0EE008l3 (2011)
[ 19] J. Liu, Z. Zhao, C. Xu, et al., Catal. Letters 120 (2008) 148; J. Phys Chem. C 112 (2008) 5930
76

NOEA 2011
Zakopane 4-7 September 2011
CIO
##### Catalytic filters for the simultaneous removal of soot and NOX: influence of the alumina precursor on monolith washcoating and catalytic activity
##### M. E. GALVEZ1, S. ASCASO1,1. TOBIAS1, R. MOLINER1, M. J. LAZARO1
^Tnstituto de Carboquimica, CS1C, Miguel Luesma Castan,
4. 50018 Zaragoza (Spain), e-mail: mlazaro@icb.csic.es
Due to their optimal fuel economy and excellent durability, the demand for light-duty diesel vehicles has increased notably in the last years, this trend expected to continue in the near term future [1,2]. The design of the combustion process in diesel engines does, however, result in high emission of particulate matter, i.c. soot. Engine modifications have helped to lower the emission of particulates in diesel engines, conforming the previously existing legislative demand. Still, there is a trade-off between the reduction of particulate matter emission and nitrogen oxides (NOX) control. Thus, the use of after- treatment technologies is required, and each time more efficient technologies are being hunted in order to meet the upcoming emission standards [3]. Under typical lean-bum operation conditions of diesel engines, three-way catalysts are not efficient in reducing NOX [4,5]. One of the latest research efforts focuses on the simultaneous elimination of both contaminants, by means of catalytic filtration of the exhaust gas. Bi-metallic alumina-supported catalysts consisting of Cu, Co and V oxides, together with alkali promoters, namely K, have shown outstanding activity in both soot oxidation and NOX reduction at temperatures from 250-650°C [6], even when the catalytic material was supported onto structured materials, such as cordierite honeycomb monoliths [7]. However, textural properties of the catalytic layer, which are strictly dependant on the type of alumina precursor employed, might influence the extent and uniformity of monolith coating, reactant diffusion towards the catalytically active sites as well as soot-catalyst contact, determining the activity of the catalytic filter in the simultaneous removal of soot and NOX.
Cordierite monoliths (2MgO-2AI2O3-5SiO2, Coming, 400 cpsi) were selected as filtering material. Several AI2O3 gels were synthesised by sol-gel synthesis. Disperal, Disperal 20, Disperal 40 and Disperal 60 (Sasol GmbH), differing in powder surface area, particle and dispersed particle size, were used as the alumina precursors. Concentrated nitric acid was added as peptizing agent. Metals and K were incorporated to the mixture by means of Cu(NO3)2-3H2O, Co(NO3)2-6H2O and NH4VO3 and KNO3. Cylindrical shaped monoliths (1x2.5 cm) were subjected to oxidation in concentrated HNO3 for approximately 5 minutes. Coating was performed by forced circulation of the gels through the channels of the cordierite monoliths, using a peristaltic pump. After 30 minutes, the coated monoliths were dried in a rotating oven at a temperature of 65°C for 24 h, and further subjected to calcination at 450°C during 4 h. Physical and chemical characterization was carried out by N2 adsorption, XRD, SEM-EDX and temperature programmed reduction (TPR). A carbon black, CB (Cabot, Elftex 430) was used as model compound of soot. The coated monolith was introduced into a dispersion of 0.2 g of CB in 180 mL of n-penlane, stirred for I min and dried at 65°C for 1 hour. The catalytic activity of the filters in the simultaneous removal of CB and NOX was tested in a fixed-bed bench-scale apparatus. A reactant gas containing 600 ppm NO-5% O2 in Ar was flowed at 50 mL/min through the catalytic filter, corresponding to a gas residence time of approximately 2.5 seconds. Dynamic experiments were performed at temperatures between 250 and 650°C, using a healing rate of 5 K/min. Concentrations in the exiting gas were analyzed in a mass spectrometer (Balzers 422) and by gas chromatography (HP 5890).
The catalytic fillers prepared substantially differed in textural and morphological features, depending on the type of precursor employed in their preparation. Properties of the different alumina gels prepared were as well strongly influenced by the alumina precursor, i.e. suspensions containing Disperal 60 (D60) gelified poorly due to much higher dispersed particle size (350 nm) in comparison with other alumina precursors (D: 80 nm, D20: 150 nm, D40: 300 nm). Viscosity increases in the order D>D20>D40>D60.
77

NOEA 2011
Zakopane 4-7 September 2011
As a result, cordierite monoliths coated using D60 were non-uniformly covered by a thinner catalytic layer; uncoated monolith channels were observed by means of SEM-EDX whereas at some points agglomeration of material was observed. On the other had, coating using the gels prepared using 1)60 and 1)40 led to catalytic layers presenting less number of cracks in comparison to I) or 1)20, as can be observed in Eig. I. Layer adherence thus notably improved by means of using 1)60, 1)40 or even 1)20 with respect to I). Textural properties determined from N2 adsorption isotherms evidence higher surface areas for the catalytic filters prepared using D, as shown in Table 1 for the particular case of a the catalytic filter 6/0.04/5:10/Co. Pore size increases in the order D60>D40>l)20>I), whereas VBJH, corresponding to mesopores, decreases following the opposite trend. While less number of cracks are formed, D40 and 1)60 resulting in non-uniform coverage of the monolith surface leave totally or partially uncovered a greater part of the original macroporous structure of the cordierite material.
Table I. Surface area, total and mesopore volume, and average pore diameter, for 6/0.04/5:10/Co, prepared using the different alumina precursors.
	D60	D40	1)20	1)
.S'B,.;7- (m2/g)	2.3	3.1	5.6	12.4
V„ (cm3/g)	0.021	0.027	0.026	0.026
VHJH (em’/g)	0.021	0.028	0.027	0.027
<Z„(nm)	64.4	34.2	15.5	6.1

Figure I. SEM images obtained for the catalytic filters 6/0.04/5:10/Co prepared using I) and 1)40 as alumina precursors
As previously reported |7|, catalytic filters show two maxima of N()x reduction, one at temperatures between 250 and 400°C, which could be associated to nitrate adsorption on K sites, and a second one, centred at about 520°C, which follows a peak of NO2 evolution and corresponds to maximal soot oxidation rate. In some cases, NOX conversions, completely selective to N2, higher than 60% were measured, particularly for the catalytic filters prepared using 1)20 as precursor. This fact points out to an optimal combination of alumina particle size leading to optimal coverage, less tendency towards crack formation, and porosity of the deposited catalytic layer, favouring catalyst-soot-reactant gas contact and diffusion. Fig. 3 depicts this observation; catalytic filters prepared using 1)20 and 1)40 yielding higher N()x conversions than D and 1)60.
78

NOEA2011
Zakopane 4-7 September 2011
Figure 2. Simultaneous removal experiment in the presence of the catalytic filter 5/0.1/5:10/Co, prepared using Disperal 20
Figure 3. NOX removal for the catalytic filters 6/0.04/5:10/Co prepared using the different alumina precursors
Authors acknowledge AECl (A/18200/08, A/9858/07), Gobiemo de Aragón-La Caixa (GA-LC- 030/2008), M.E. Galvez is indebted to the Spanish Ministry of Science and Innovation for her Juan de la Cierva post-doctoral fellowship. S. Ascaso acknowledges CSIC for her JAE pre-doctoral grant
[11 RJ. Farrauto, K.E. Voss, Appl. Cat. B 10 (1996) 29
79

NOEA2011
Zakopane 4-7 September 2011
1. J. Aller, Int. J. Appl. Ceram. Technol. 2 (2005) 429
2. Regulation (EC) No. 715/2007
3. D. Fino, N. Russo, C. Baldini, G. Saracco, V. Specchia, AIChE J. 8 (2003) 2173
4. P. Ciambelli, P. Corbo, F. Migliardini, Cat. Today 59 (2000) 279
5. M.E. Galvez, S. Ascaso, I. Suelves, R. Moliner, R. Jimenez, X. Garcia, A. Gordon, MJ. Lazaro, Cat. Today (2010), in press, doi: DOI: 10.l016/j.cattod.2010.l 1.045
6. M.E. Galvez, S. Ascaso, R. Moliner, R. Jimenez, X. Garcia, A. Gordon, MJ. Lazaro, Cat. Today (2011), in press, doi: 10.1016/j.cattod.20l 1.01.030

NOEA2011
Zakopane 4-7 September 2011
Cli
##### Silver-based catalysts for NOX SCR with ethanol: a mechanistic study on Ag/ZSM-5 and Ag/A^Oj
##### A. WESTERMANN1, R. BARTOLOMEU23, B. AZAMBRE1, R. BERTOLO2,
##### C. HENRIQUES2, A. KOCH1, P. Da COSTA3, M. F. RIBEIRO2
1. Laboratoire de Chimie et Methodologies pour I’Environnement (LCME), Institut Jean-Barriol, Universite Paul Verlaine de Metz - Rue Victor Demange, 57500 Saint Avoid, France
2. instituto Superior Tecnico, Institute for Biotechnology and Bioengineering,
Centre for Biological and Chemical Engineering, Av. Rovisco Pais, 1049-001 Lisboa, Portugal
Universite Pierre et Marie Curie, CNRS UMR 7190, 78210 Saint Cyr I'Ecole, France
Environmental regulations on NO, emissions of mobile sources are becoming increasingly demanding. Therefore, catalytic after treatments such as NO,-SCR must be further developed. One of the possible reducers that can be employed for NO,-SCR is ethanol: it is environmental friendly and can be produced from renewable sources. Ag/Al2O3 catalysts have been reported in the literature to be highly active for this system [1,2]. Although less active, silver-containing zeolites are promising catalysts and have attracted much interest. It is believed that through in-depth studies it will be possible to understand the differences between these two types of systems.
In this work, Temperature Programmed Surface Reactions (TPSR) and DRIFTS studies of NO, SCR with ethanol were performed on Ag/AI2O3 and Ag/ZSM-5 catalysts in order to assess the fundamental differences in the intermediates produced by each catalyst and propose a mechanism for each catalytic system.
Commercial ZSM-5 zeolite with Si/Al = 25 was provided by Zeolyst. Ag/ZSM-5 zeolite was prepared by a threefold ion-exchange with a 0.01 M AgNO3 solution. Then, it was calcined under air at 500°C for 8 h. Commercial y-Al2O3 spheres (SBET = 170 m2/g ) were provided by Sasol. Ag/Al2O3 was prepared by excess solvent impregnation with an AgNO3 solution. The spheres were then calcined under air at 500°C for 2 h and crushed into a fine powder. Silver content in Ag/ZSM-5 and in Ag/Al2O3 catalysts was determined by chemical analysis and was found to be 4.1 and 2.5 wt.%, respectively.
The characteristics of silver species in both catalysts were investigated using TEM, H2-TPR, in situ DRS spectroscopy, and DRIFTS of adsorbed CO.
Catalytic tests under isothermal or ramp (TPSR) modes and operando DRIFTS studies were performed on both catalysts, previously pre-treated at 500°C under He/O2. under the following conditions:
NO (1900 ppm), EtOH (3020 ppm), O2 (5 %); (ii) NO2 (1590 ppm), EtOH (3020 ppm); (iii) EtOH (3020 ppm). For the SCR tests, the detection/quanlificalion of the gaseous N- and C-reactants/products (more than 10) at the outlet of the fixed bed reactor was done using a cyclone FTIR gas cell (2 m) coupled to a Varian Excalibur 4100 FTIR spectrometer. The nature of adsorbed intermediates was investigated using a Graseby Specac "the selector" DRIFTS optical accessory and a Spectra-Tech environmental cell.
First, the catalytic activities of Ag/Al2O3 and Ag/ZSM-5 on NO, SCR with ethanol were measured under isothermal or TPSR standard conditions. As expected, isothermal NO, conversion was near 100% in the 300-400°C range for the benchmark Ag/AI2O3 catalyst, whereas it was limited to 56% at about 400°C for Ag/ZSM-5. In both cases, the DeNO, window was found to be relatively broad (especially for Ag/Al2O3) due to the presence of several secondary reductants formed by the catalyzed or non-catalyzed partial oxidation (acetaldehyde, acetic acid, CO, formaldehyde...) and/or dehydration (ethene, diethylether) of ethanol over a wide range of temperatures. This is in line with our previous studies on ceria-zirconia catalysts [3], Owing to the presence of Bronsted acid sites on the zeolite, selectivity to C- or N-products was found to differ between both catalysts, with more ethene, less acetaldehyde and reactive nitrates and a higher CO/CO2 ratio for Ag/ZSM-5. The formation of ethene is thought to be detrimental for DeNO, activity because it is: (i) a less selective reductant than acetaldehyde; (ii) a well known precursor of coke. By contrast, the Ag/Al2O3 catalyst, only containing Lewis acid sites and basic properties, rather promotes
81

NOEA2011
Zakopane 4-7 September 2011
the enolisation of acetaldehyde, as revealed by DRIFTS. These enolate species were found to be highly reactive with NO2 and are thought to be key surface C-intermediates for the formation -NC and -NCO species and amine-like species, yielding N2 by pathways rather similar to NH3-SCR (Fig. 1).
Figure 1. Possible reaction scheme over silver-catalysts for SCR with ethanol.
The selectivity towards the different C- and N- products, especially acetaldehyde and its derived species can be influenced by the electronic state of silver species and their reducibility which, according to the characterisation results, depend on the nature of the catalyst support.
The temperature dependence of the state of Ag species under SCR conditions and the existence of different populations of some adsorbed and gaseous intermediates can explain the slightly different behaviours observed, especially at 250°C. On the fresh catalysts (TPSR runs), ethoxy (C2H5O) species and ethylnitrite (C2H5ONO) were formed in high amounts at low temperatures [3], whereas under steady state conditions (isothermal tests), the SCR reaction was somewhat hindered by the accumulation of rather stable C-products such as acetates and/or coke oligomers, which are not involved in the formation of N2.
In absence of O2 (NO2+EtOH), the NOK conversion decreased from 100% to 50% on Ag/Al2O3 catalyst and slightly less for Ag/HZSM-5. This indicates the key role of O2 in preventing the accumulation of undesirable C- and N- ad-species on the surface. Moreover, the presence of O2 was beneficial to avoid the polymerization of -C=N and/or -C=N=O species (to triazine- or melamine-like products) on Ag/Al2O3, which arose above 310°C under NO2+EtOH conditions and are believed to hinder DeNOx activity by blocking the active sites.
A possible reaction scheme, based on the above findings, is proposed in Fig. 1.
1. A. Musi, P. Massiani, D. Brouri, J.-M. Trichard and P. Da Costa, Catal. Lett. 128 (2009) 25
2. S. Kameoka, Y. Ukisu and T. Miyadera, PCCP 2 (2000) 367
3. A. Westermann, B. Azambre, Catal. Today (2010) doi: 10.1016/j.cattod.2010.10.071
82

NOEA20II
Zakopane 4-7 September 2011
C12
##### Investigation of Cs-Cu/ZrCh systems for simultaneous NOX reduction and carbonaceous particles oxidation
##### A. AISSAT13, D. COURCOT1-2*, S. SIFFERT1-2
1. Univ Lille Nord de France, F-59000 Lille, France
2. ULCO, UCEIV, F-59140 Dunkerque, France
Corresponding author: courcot@univ-littoral.fr, Tel.: +33-328658237 (D. Courcot)
Copper based catalysts have been widely studied either in hydrocarbons and soot oxidation [ I -4] or in reduction of NO, [2,5,6]. The use of an alkali and copper showed a synergy between the two metals in the oxidation of carbonaceous particles named carbon black (CB) [2], Cu/ZrO2 systems also showed good performances in NOX reduction in the presence of hydrocarbons [7], Thus, the use of Cs-Cu/ZrO2 systems in simultaneous NO reduction and soot oxidation could be an avantageous route for pollutants abatements from stationary or mobile sources. The aim of this work has been focused on the catalytic properties of Cs-Cu/ZrO2 and the influence of Cs content towards the activity for both CB oxidation and NO, reduction.
Cs-Cu/ZrO2 solids were prepared by impregnation or co-impregnation of Cs2CO3 and/or CuCO3 nCu(OH)2 salts onto ZrO2 support beforehand obtained according to Hleis et al. [7]. After drying, the samples were calcined under air flow at 600°C for 4 h. The as-obtained solids were denoted Csx-CUy/ZrO2, where x (0.03 or 0.15) and y (0.1 or 0.2) correspond to Cs/Zr and Cu/Zr atomic ratios respectively. The catalysts were characterized by BET surface measurements, XRD, TPR and FTIR. Printex U was chosen as a model of carbonaceous particles for oxidation test. CB oxidation was first carried out in a continuous flow reactor (10%O2/N2, 100 mL min'1) using 100 mg of the catalyst and 6 wt% of CB. Simultaneous NO, reduction and CB oxidation were also performed using the test apparatus (6wt% CB, 900 ppm of NO/N2 + 10% O2/N2, 100 mL min'1). The volume hourly space velocity (VHSV) was 105 000 h1.
Catalytic tests results show that the CB oxidation is favoured in the presence of cesium, which increases the contact between carbonaceous particles and the catalytic surface [7], Oxidizing properties of NO, in CB elimination is clearly evidenced by values of Tmax (temperature at which CB oxidation rate is maximum) shifted towards low temperature (Table 1). Simultaneously, the maximum of NO, conversion is detected in the same temperature and higher amounts of NO, are found to be converted in the presence of cesium. Some explanation could be provided from further tests (Fig. 1). It has been evidenced that Cu-Cs/ZrO2 are able to form NO2, which appears as a step prior to its participation as a strongly oxidizing agent in CB elimination. Moreover, in the case of Cs-Cu/ZrO2 with high Cs content, it has been also shown from FTIR measurements that the catalyst is able to form NO< surface species partly involved in the oxidation of CB.
XRD characterization showed that the increase in the amount of Cs leads to the formation of a higher proportion of CuO aggregates which are active for CB oxidation. TPR measurements [8] showed also that the presence of Cs strongly affects the reduction behaviour of Cu(II) due not only to the change in Cu(II) species but also the interaction between cesium and copper oxide. These features account for an increased participation of Cu(ll) species in the oxidation of soot via a redox mechanism [9],
83

NOEA 2011
Zakopane 4-7 September 2011
Table I. Temperature at which CB oxidation rate is maximum (Tmlx) and NOX conversion values
Catalyst	Tmax CB oxidation (°C)
10% o2 no+io%o2	NO, conversion max. (%)
Cso.i5-Cuo.|/Zr02	321	355	25.9 (at 370°C)
Cso.o3-Cuo j/ZrOj	482	383	22.8 (at 391 °C)
Cu0.|/ZrO2	498	405	16.3 (at410°C)
C'Sy 15-CUo 2/Z1O2	330	354	19.1 (at368°C)
Cso.o3"Cuo.2/Zr02	484	382	19.1 (at393°C)
Cuo2/Zr02	485	405	9.1 (at404°C)

Figure 1. Outlet concentration of NO and NO2for Cs0 /S-Cuo i/ZrO2 and Csddj-Cuu//rO2 catalysts: (A) blank test without CB, (B) test in the presence of CB (a: NO2, b: NO and c: NOX).
The “Nord-Pas de Calais" Region, the "Syndicat Mixte de la Cote d'Opale” and European Union via Interreg IV "Redugaz project" are gratefully acknowledged for financial support.
1. C.-C. Chien, T.-J. Huang, Ind. Eng. Chem. Res. 34 (1995) 1952
2. I.D. Lick, A.L. Carrascull, M.I. Ponzi, E.N. Ponzi, Ind. Eng. Chem. Res. 47 (2008) 3834
3. J.P.A. Neeft, M. Makkee, J.A. Moulijn, Chem. Eng. J. 64 (1996) 295
84

NOEA 2011
Zakopane 4-7 September 2011
1. D. Pietrogiacomi, D. Sannino, S. Tuti, P. Ciambelli, V. Indovina, M. Occhiuzzi, E Pepe, Appl. Catal. B21 (1999) 141
2. M. Karthik, L.-Y. Lin, H. Bai, Microporous Mesoporous Mater. 117 (2009) 153
3. V.I. Parvulescu, P. Grange, B. Delmon, Catal. Today 46 (1998) 233
4. D. Hleis, M. Labaki, H. Laversin, D. Courcot, A. Aboukai's, Colloids Surf. A 330 (2008) 193
5. A. Aissat, D. Courcot, R. Cousin, S. Siffert, Catalysis Today DOI: 10.1016/j.cattod.2011.01.033 (2011)
6. H. Laversin, D. Courcot, E.A. Zhilinskaya, R. Cousin, A. Aboukai's, J. Catal. 241 (2006) 456

NOEA2011
Zakopane 4-7 September 2011
C13
##### Effect of water on NO decomposition over Cu-ZSM5 based catalysts
##### G. LANDI1, L. LISI1, R. PIRONE1 2, G. RUSSO3 4, M. TORTORELL13
1 Istituto di Ricerche sulla Combustione - CNR, P.le Tecchio 80, 80125, Naples,Italy
2 Dipartimento di Scienza dei Materiali e Ingegneria Chimica del Politecnico di Torino,
Corso Duca degli Abruzzi 24, 10129, Torino, Italy
Dipartimento di Ingegneria Chimica delTUniversita di Napoli Federico II,
P.le Tecchio 80,80125, Naples, Italy, e-mail: miriam.tortorelli@unina.it
The catalytic decomposition of NO into N2 and 02 represents the ideal process to remove nitrogen oxides in the presence of oxygen. Cu-exchanged ZSM5 zeolite is the most promising catalyst for this process and, although several limitations hinder practical applications, it was widely investigated to understand its unique behaviour of this zeolite [1,2], One of the main drawbacks is the presence of water vapour in the feed which causes deactivation generally associated to copper shifting to inactive positions. Rare earth ions addition was reported to be effective to partially prevent catalyst deactivation [3].
In this study the effect of water vapour on the adsorption and decomposition of NO was studied by conducting adsorption, TPD and NO decomposition tests on both pre-reduced Cu-ZSM5 and LaCu-ZSM5 catalysts. The adsorption experiments were carried out at I25°C in the presence or in the absence of H2O in the NO/He feed mixture. The original catalytic activity towards NO decomposition is totally recovered when waler, previously adsorbed at low temperature, is desorbed before starting the reaction at 450°C. This result rules out the hypothesis that water could deactivate the catalyst even al low temperature. Nevertheless, the co-adsorption of water dramatically decreases the amount of adsorbed NO at 125°C under dry conditions. The addition of lanthanum to a Cu-ZSM5 catalyst increased the amount of NO adsorbed in the absence of water and significantly limits the decrease of NO adsorption in the presence of water. TPD experiments carried out after NO adsorption showed that the addition of lanthanum promotes the formation of nitrates which are considered as reaction intermediates in the NO decomposition [4].
[1]	V. I. Parvulescu, P. Grange and B. Delmon, Catal. Today 46 (1998) 369
[2]	H. Yahiro and M. Iwamoto, Appl. Catal. A222 (2001) 163
[3]	B. I. Palella, L. Lisi, R. Pironc, G. Russo, M. Notaro, Kinel. Catal. 47 (2006) 728
[4]	E Garin, Appl. Catal. A 222 (2001) 183
87

NOEA 2011
Zakopane 4-7 September 2011
C14
##### Hysteresis effect study on Diesel Oxidation Catalyst for a better efficiency of SCR systems
##### A. MANIGRASSO1’2, N. FOUCHAL1, P. DARCY2, P. Da COSTA*
1 Universite Pierre et Marie Curie, Institut Jean le Rond d’Alembert, 2,
Place de la Gare de Ceinture 78210 Saint-Cyr I'Ecole, France
2 RENAULTS.A.S., FR.TCR.LAB.012, 1 avenue du Golf,
78288 Guyancourt Cedex, France, alexis.manigrasso@renault.com
This study is focusing on the behaviour of the DOC in order to improve the efficiency of an ammonia SCR system on a after-treatment line composed by a DOC + DPF + SCR. As it's known [1], the control of the NO2 before the SCR system is very important and in case of the hybridization of the vehicle, this control is affected by a hysteresis effect.
The hybrid power technologies have been applied successfully in vehicles [2], With the combined use of two different powertrain technologies, the hybrid vehicles can work with high efficiency, low pollutants emission and fuel consumption. An example of this application can be the hybridization between and internal combustion engine and an electric powertrain. In this case, the after-treatment system (like the Diesel Oxidation Catalyst, DOC) used operate under a transient temperature profile who lead to an hysteresis behaviour in the catalytic activity during heat-up phases and cool down phases [3]. The most likely explanation for the observed hysteresis effect is a reversible oxidation of the catalyst surface.
The commonly accepted explanation for the reversible deactivation by oxidative treatments is an oxide formation of the platinum. The formation of such surface oxides has been demonstrated by a number of experimental techniques [4]. The nature of the platinum oxides does not seem to be fully understood, possible candidates can be subsurface oxygen [5,6], formation of a platinum oxide layer [7] or even the bulk oxidation of the platinum panicles.
In this paper we’ll study the NO, CO and HC oxidation process under different temperature cycles composed by light-off followed by light-down conditions. The main objective of this paper is to demonstrate that even with a constant exhaust composition and hysteresis effect on a commercial catalyst can be observed and explained.
The catalyst is a commercial diesel oxidation catalyst (Pt/Pd/AI2O3). For this study, sample catalyst is extracted from a monolith and different ageing of the catalyst were used. Before runs and characterization, the carrots were calcinated in industrial air (Ar) at 500 °C for 1 h, using a heating rate of IO°Cmiri'.
The catalyst, were characterized by elementary analysis, X-ray diffraction (XRD), transmission electron microscopy (TEM) and by X-ray Photoelectrons Spectroscopy (XPS). The specific surface area was also calculated using a specific apparatus. Main physicochemical properties and elementary analysis of the catalysts was performed by the “Service Central d’Analyses du CNRS” in order to determine the noble metal contents.
Each study was performed in temperature programmed surface reaction (TPSR). The heating rate was chosen equal to IO°C min '.The TPSR were used to determine light off temperature of each pollutant present in the exhaust gases [8-9], To be close to industrial conditions, our experimental setup is composed by an heater were the gases are heated up to 500°C. These hot gases flowed through the catalytic bed composed by the sample catalyst. Three thermocouples are available to follow the reaction temperature. One is place before the catalyst, the second one close to the catalyst and the third at the exit of the reactor (at 10 cm from the catalyst). The temperatures given in this study are those obtained close to the catalyst. The gas hourly space velocity (GHSV) was chosen equal to 25,000 h1.
During the light-off/lighi-down-experiments the temperature was increased from 80 to 500°C with a heating rate of 10°C min'1. After reaching 500 °C it was cooled to 80°C with an applied rate
89

NOEA 2011
Zakopane 4-7 September 2011
of 10°C min'1 2 3 4 5 6 7 8 9. This sequence of heating and cooling will further be referenced as runl. This cycle of heating and cooling was repeated without further pre-treatment (run 2). During the heating and cooling phases the feed gas composition was held constant. 1 2 3 4 5 6 7 8 9
Figure 1. Shows a hysteresis in the NO conversion between heat-up phase and cooling down phase, this point can be explain by a reversible oxidation of the platinum particles. At high temperatures platinum is oxidized by NO2 or O2 to form an oxide (PtO2) that is more active than the metallic platinum particle. At lower temperatures the particle would be reduced back to its original state, most likely by NO.
[1]	A. Grossale, I. Nova, E. Tronconi, Journal of Catalysis 265 (2009) 141
[2]	A. Emadi, K. Rajashekara, Special section on hybrid electric and fuel cell vehicles, IEEE Transactions on Vehicular Technology 54 (3) (2005) 761
[3]	W. Hauptmann, M. Votsmeier, J. Gieshoff, A. Drochner, H. Vogel, Appl. Catal. B 93 (2009) 22
[4]	L. Olsson, E. Fridell, J. of Catal. 210 (2002) 340
[5]	H. Niehus, G. Comsa, Surf. Sci. 93 (1980) L147
[6]	A. von Oertzen, A. Mikhailov, H.H. Rotermund, G. Ertl, Surf. Sci. 350 (1996) 259
[7]	R.W.McCabe,C.Wong,H.S.Woo,J.ofCatal. 114(1988)354
[8]	K.C. Taylor, A. Crucq, A. Frennet (Eds.), Catalysis and Automotive Pollution Control, Elsevier, Amsterdam, 1987, p. 97
[9]	J. Barbier Jr., D. Duprez, Appl. Catal. A 85 (1992) 89
90

NOEA 2011
Zakopane 4-7 September 2011
K13
##### Low temperature N2O decomposition over nano oxide catalysts
##### A. KOTARBA1, G. MANIAK1, P. STELMACHOWSKI1, W. PISKORZ1,
##### F. ZASADA1, Z. SOJKA1
1 Jagiellonian University, Cracow, 30-060, Poland
Nitrous oxide is a greenhouse gas with global warming potential 310 times higher than CO2. Since the N2O amount emitted from nitric acid production plants will be taxed starting from 2013, the intensive research is focused on development of efficient N2O abatement catalysts. Clearly, catalytic methods will play a crucial role in elimination of N2O from exhaust gases. In this context catalytic properties of a vast range of materials have been explored, such as supported metals, simple and complex oxides, as well as metal exchange zeolites. However, none of the many catalysts developed until now exhibit satisfactory performance in real low temperature deN2O process conditions.
In this paper exploration of the mechanistic pathways of N2O decomposition over various oxide catalysts by means of experimental (microscopic, spectroscopic, kinetic) investigations and molecular modeling will be presented. The comparison between the catalytic activity in deN2O reaction of alkaline earth metal oxides (via anionic redox mechanism) and d metal oxides (via cationic redox mechanism) will be addressed. Emphasis will be placed on the surface morphological irregularities, which are present inevitably on nano-oxide materials.
The paper illustrates how combined experimental and molecular modeling approach provides rational strategies for development of promising catalytic materials for practical applications. The optimization of the deN2O catalyst will be discussed in terms of structural doping of the oxide materials, control grain morphology and tuning of the electronic properties by surface doping.

NOEA2011
Zakopane 4-7 September 2011
C15
##### The influence of structural promoters on the activity of iron oxide-based catalyst for N2O decomposition
##### P. KOWALIK1, K. STOLECKI1, K. MICHALSKA1, J. KRUK1, M. KONKOL1
1 Fertilizers Research Institute, Catalyst Department, Puławy, Poland
Nitrous oxide, (N2O) is a harmful gas, contributing to the greenhouse effect (310-times stronger than CO2) and ozone layer depletion. There are two sources of N2O formation: natural processes and industrial activity - mainly nitric acid production [1,2], In the course of ammonia oxidation process a part of ammonia is converted into nitrous oxide. High-temperature decomposition of N2O in catalytic bed placed under platinum alloy gauzes is the simplest way of N2O removal. Iron-based catalysts are known to be effective for direct N2O decomposition in high temperature region [3,4], The aim of our research is to investigate the effect of modifiers on activity and physicochemical properties of iron oxide-based catalysts.
Model samples containing the same amount of Fe2O3 (80% wt.) with different kind of structural promoter (oxides of: Al, Zr, Ce, La, Cu or Cr) were precipitated by addition of an aqueous solution of ferrous sulfate and a nitrate of one of the modifiers to the sodium hydroxide aqueous solution at 80°C with the final pH value of 10. The precursor materials obtained were filtered, dried and then calcined at 650°C for 3h.
Activity determination was done in a quartz Zielinski-type reactor [5] in the temperature range of 500-900°C. A catalyst sample (50-100 mg) grounded to the fraction of 0,16-0,25 mm placed into the reactor was loaded with feedstock containing 1500 ppm N2O, 1500 ppm NO and N2 as an inert. Decomposition rate was determined on the basis of the N2O concentration in the outlet gases.
The XRD analysis showed that hematite is a dominant phase in all catalysts. Specific surface area is in the range 20-50 m1 2 3 4 5/g, and after high temperature treatment at 900°C it decreases to 10-20 m2/g.
A distinct influence of the modifier type on the catalytic activity of iron oxide in the N2O decomposition process was observed. The correlation between decomposition rate and temperature shows that the catalyst modified with La, Cu or Al degrade N2O already at a temperature slightly higher than 600°C, whereas for Zr- and Ce-modified catalysts decomposition occurs at 700°C. The Fe2O3/Cr2O3 catalyst exhibits the highest initial temperature for N2O decomposition in the temperature range interesting from the practical point of view the catalytic activity was found to increase in the following order: La>AI>Cu>Zr>Ce>Cr.
The Fe2O3/CuO catalyst has higher activity for N2O decomposition than the Fe2O3/AI2O3 system at the temperature of 800°C. Moreover, at 900°C higher activity was observed for the La-modified catalyst.
[1]	R. T. Ellington, M. Meo, Chem. Eng. Prog. 7 (1990) 58
[2]	J. Perez-Ramirez, F. Kapteijn, K. Schoffel, J. A. Moulijn, Appl. Catal. B 44 (2003) 117
[3]	A. Gołębiowski, J. Kruk, M. Wilk, Investigation of N2O Catalytic Decomposition at High Temperature, International Symposium on Air Pollution Abatement Catalysis 2005, Cracow, Poland
[4]	G. Giecko, T. Borowiecki, W. Gac, J. Kruk, Catal. Today 137 (2008) 403
[5]	J. Zieliński, React. Kinel. Catal. Lett. 17 (1981) 69
93

NOEA2011
Zakopane 4-7 September 2011
C16
#### Stoichiometric and non-stoichiometric Perovskite-based catalysts for the catalytic decomposition of N2O from nitric acid plants Y. WU1, X. NI\ P. GRANGER1, C, DUJARDIN1
1 University Lille Nord de France, Unite de Catalyse et de Chimie du solide,
CNRS UMR 8181, City Scientifique, Batiment C3, 59655, Villeneuve d’Ascq, France,
e-mail: christophe.dujardin@univ-lillel.fr
There is a growing interest to minimize the emissions of nitrous oxide (N2O) as side-product from nitric acid plants due to a global wanning potential of approximately 300 times higher than that of CO2 [1]. Different strategies have already been implemented at industrial scale but they are still suffering from significant drawbacks essentially associated to a poor selectivity and sometimes a short lifetime in particular when the catalytic process is inserted downstream the ammonia burner. Previous in-situ XRD measurements performed in our laboratory revealed the excellent thermal stability of perovskite based catalysts in the presence of water vapor at high temperature [2], which suggests its potential application for the decomposition of nitrous oxides from nitric acid plants. The non-stoichiometric perovskite-based catalysts were examined in order to investigate a possible support effect of segregated oxides on perovskite that could enhance or lower die catalytic activity subsequently. An additional aspect has to be taken into account associated with the catalyst selectivity because the decomposition of NO must be avoided to preserve the cost efficiency of those typical industrial plants.
Two series of stoichiometric and non-stoichiometric Perovskite-based catalysts (LaCO|.yO3±)L and I^i-xCoojFeojO^ were synthesized according to a conventional sol-gel method involving a citrate route [3]. Precursors thus obtained were dried overnight at 80 °C then calcined in air at 600°C or 900 °C for 8 h. The prepared catalysts were characterized by BET, XRD, Raman, H2-TPR and XPS. Temperature­programmed experiments were performed in a fixed-bed flow reactor using 0.7 g of catalyst with a total flow of 15 L.h ’ within a temperature range between 20 and 900 °C. The reactant mixture was typically composed of 0.1 vol.% N2O, 5 vol.% NO, 6 vol. % O2, 15 vol. % H2O and balanced by He. A second catalytic test was performed after ageing overnight at 900°C under reactant mixture in order to characterize the stability of our catalysts.
95

NOEA2011
Zakopane 4-7 September 2011
The XRD patterns recorded on the catalysts evidence the rhombohedral structure of LaCoO3 and a slight segregation of La2O3 on LaCo1.yO3±x samples that could be related with the increase of specific surface area up to 12 m1 2 3/g (LaCoo.803 calcined at 900°C). For Lai.JCo08Fe02O3±>. samples, a progressive segregation of cobalt oxide is revealed with decreasing lanthanum stoichiometry but the specific surface area remains almost unaffected. The reducibility of these series of catalysts is examined by using H2-temperature-programmed reduction. The typical profile related to H2 consumption exhibits 2 domains of reduction, the reduction of Co3+ into Co2+ around 300-450°C and the subsequent reduction of Co2+ into Co0 above 500°C in agreement with H2 consumption [3]. The modification of stoichiometry slightly changes the reducibility accompanied with a shift of temperature T^ for both domains. The characterisation of solids clearly evidences the formation of perovskite structure and the segregation of either La2O3 that enhances the specific surface area for LaCol yO3±x or the preferential segregation of Co^ in the case of La1.ICo0 8Fe0 2O3±x solids. We pay a special attention to a possible support effect that could involve the stabilisation of active phase. The Figure 2 compares the catalytic activity for the N2O decomposition into N2 for the freshly calcined catalyst and the catalyst aged under reaction conditions at 900°C overnight. For all the samples, they show an exclusive selectivity towards N2O decomposition without NO loss. A strong activity enhancement in N2O conversion is observed on the substituted sample (LaCoo8Feo,203) and the introduction of iron on LaCoO3 leads to a stabilisation of the solid revealed by a decrease of the deactivation after ageing. This synergy effect is correlated to the improvement of oxygen mobility which agrees with the observation of H2-TPR. Moreover after ageing procedure, the catalytic activity of Lao.ęCoo 8Feo.203±3. sample remains higher than stoichiometric one. The influence of the support and on the nature of segregated oxide will be discussed during the presentation.
Figure 2: Comparison of N20 conversion curves of Lai.xCoQgFeo203^ of fresh sample and after ageing overnight under 0.1 %N20+5%N0+6%02+15%H2O +He
[1]	J. Pćrez-Ramirez, E Kapteijn, K. Schoffel, J.A. Moulijn, Appl. Catal. B 44 (2003) 117
[2]	S. Muller, J.P. Dacquin, Y. Wu, C. Dujardin, P. Granger, P. Burg, Catalysis Today, DOI: CATTOD- D-10-00453R1
[3]	I. Twagirashema, M. Engelmann-Pirez, M. Frere, L. Burylo, L. Gengembre, C. Dujardin, P Granger, Catal. Today 119 (2007) 100
96

NOEA201I
Zakopane 4-7 September 2011
KI4
##### N2O catalytic decomposition - from laboratory experiment to industry reactor
##### L. OBALOVA1,2, K. JIRATOVA3,F. KOVANDA4
VŚB - Technical University of Ostrava,
1 Faculty of Metallurgy and Materials Engineering
1 Centre for Environmental Technologies, 17. listopadu 15,
708 33 Ostrava, Czech Republic
3 Institute of Chemical Process Fundamentals CAS v.v.i., Rozvojova 135,
165 02 Prague, Czech Republic
4 Institute of Chemical Technology, Department of Solid State Chemistry, Technicka 5,
160 00 Prague, Czech Republic
In last years, the catalytic decomposition of N2O as a method for abatement of N2O emissions in waste gases attracts increasing attention due to the expected inclusion of N2O in the greenhouse gas trade. Many research groups are focused on the development of suitable catalysts for this reaction because it is still a problem to find the catalyst with sufficient activity and stability in real off-gas conditions due to water, oxygen and NOX inhibition effects.
Multicomponent mixed oxides prepared by thermal treatment of layered double hydroxide (LDH) precursors seem to be promising catalysis for this reaction. Layered double hydroxides with general chemical composition of |Mll|.xMl"x(OH)2|x+[Anx/n ,yH2O]x where M11 and M111 are divalent and trivalent metal cations and A"' is an n-valent anion (often carbonate) consist of positively charged hydroxide layers separated by interlayers containing anions and water molecules. Thermal treatment of LDH precursors gives finely dispersed mixed oxides of M11 and M111 with large surface area and good thermal stability.
Intrinsic kinetic data were obtained in laboratory experiments of N2O decomposition over grained LDH-related mixed oxides; these data were used for modeling of catalytic performance of catalyst particles suitable for industrial use and compared with experiment. Pseudo-homogeneous one-dimensional model of an ideal plug flow reactor in isothermal regime was applied; the effect of internal and external mass transport was described by effectiveness factor. The N2O abatement by using a catalytic reactor situated downstream the DcNOx technology in nitric acid production unit was estimated, based on laboratory data of N2O decomposition in simulated off gas from nitric acid production.
This work was supported by the Technology Agency of the Czech Republic (project No. TA 0/020336) and EU project No. CZ. 1.05/2.1.00/03.0100 „Institute of Environmental Technologies".
97

NOEA2011
Zakopane 4-7 September 2011
CI7
##### The application of metallic iron for N2O reduction at higher temperature and oxygen presence
##### J. LASEK1*, B. GRADOŃ2
1 Institute for Chemical Processing of Coal, Zamkowa 1, 41-803 Zabrze, Poland
2 Department of Metallurgy, Silesian University of Technology,
Krasińskiego 8, 40-019 Katowice, Poland
Corresponding author (J. Lasek) jlasek@ichpw.zabrze.pl
The nitrous oxide is recognized as a pollutant of known, negative impact on environment. Il is a greenhouse gas. Due to a long lifetime in the atmospheric conditions, its molecules can migrate to the stratosphere and there lake a part in the stratospheric ozone depletion. The N2O can be formed in many natural processes but substantial share to its global emission is contributed by human activities, mainly acid production, agriculture and combustion processes for production heat and electricity. The level of the N2O emission from the combustion equipments depends mainly on type of fuel and temperature. Concentrations of the N2O in the flue gases leaving industrial gaseous furnaces and pulverized coal boilers, operating al high temperatures, are very small and do not exceed 5 ppm. Nevertheless, much higher values are observed in case of the fluidized bed combustors (FBC): 20-200 ppm depending on temperature and combustion air excess. The highest emissions are observed from circulating fluidized bed boilers. On the other hand this combustion technology becomes more and more popular due to ability to utilize low-rank coals, biomass and waste with high combustion efficiency and environmentally favorable performance.
The paper presents the results of the experimental investigation of nitrous oxide reduction by reaction with metallic iron, within the temperature range of 600-850°C. Experiments were carried out in a one-dimensional tubular flow reactor externally heated in an electrical furnace. The spherical and cylindrical iron samples of well-defined and fixed surface area were placed in the center of the reactor. Mixtures of N2O/N2, N2O/O2/N2 and NO/CO2/N2 of different molar compounds fractions were continuously fed into the reactor. On basis of these experiments the intrinsic rate of the reaction between nitrous oxide and Fe in the first stage of iron oxidization was measured. The obtained results are compared with the literature data. An impact of oxygen present in reaction zone on inhibition of deN2O process has been investigated. A very strong and fast decreasing of N2O reduction was observed when more than 2 vol% O2-containing gas mixture was introduced into reaction zone. The surfaces and cross-sections of partly oxidized iron samples were observed using a scanning and light microscopes.
99

NOEA 2011
Zakopane 4-7 September 2011
C18
##### Copper ionic pairs as active sites in N2O decomposition on CuOx/CeO2 catalysts
##### A. ADAMSKI1, W. ZAJĄC13, F. ZASADA1, Z. SOJKA1
1 Faculty of Chemistry, Jagiellonian University,3 Ingardena St., PL 30-060 Cracow
1 AGH University of Science and Technology, Faculty of Energy and Fuels,
Al. Mickiewicza 30, PL 30-059 Cracow
Ceria-supported copper systems belong to the important class of heterogeneous catalysts extensively studied for both fundamental and applied reasons. Structural similarity of copper centers to those occurring in selected enzymes, particular distribution of copper species between surface and bulk, oxidative power of ceria and specific interaction of surface centers with small reactant molecules from the gas phase are responsible for still growing interest in studying such materials. One of the most important catalytic applications of ceria-supported systems can be redox processes including CO or CH4 oxidation to CO2, soot oxidation in the presence of NOX, etc. Taking into account that nitrous oxide reductase is a dimeric copper - dependent bacterial enzyme that catalyses the reduction of N2O to N2 and that copper dimers can be formed within CuOx/CeO2 systems quite easily, it could be assumed that coupled copper species constitute active sites for deN2O reaction also in the case of ceria-supported catalysts. In the current structural (XRD, SEM) spectroscopic (EPR, RS) and catalytic studies, supported by DFT calculations, the role of mono- and dimeric copper centers in deN2O reaction was elucidated. Particular attention was paid to the structure and localization of Cu2+-Cu2+ pairs in CeO2 matrix, conditions of their formation and stability.
Ceria was synthesized from O.IM aqueous solution of Ce(NO3)3 by stepwise precipitation with ammonia. Final support was calcined in air at 600°C for 6h. Copper-functionalized ceria samples, containing 5 mol. % of CuO, were synthesized in two ways: by coprecipitation with concentrated solution of ammonia or by impregnation of the CeO2 support with an aqueous solution of Cu(NO3)2. Catalysts were calcined at 600°C/6h. Catalytic tests in deN2O reaction were performed in TPSR mode with QMS detection. Quartz reactor filled with ca. 300 mg of sample was heated with the rate of 10°C/min in the temperature rangeof 20-700°C. The reactants (5 % N2O/He, 3% O2/He) flow rate of 7000 h'1 was used.
For all calculations the unrestricted DFT was chosen with use of the DMol3 program package as implemented in Materials Studio of Accelrys Inc. To describe exchange-correlation effects the functional of generalized gradient approximation (GGA) level was chosen with parametrization proposed by Perdrew et al. (PW9I). All slab calculations were performed using standart Monckhorst-Pack grid (2x2x1 sampling mesh) with Fermi smearing with o parameter set to 0.01 Ha and a cutoff energy of 4.5 A.
101

NOEA2011
Zakopane 4-7 September 2011
Figure 1. Model geometry ofCu-doped CeO2 surface.
Calculated surface energies indicate that the most stable termination of CeO2 Crystalites is (111) and thus Crystalite shape predicted via Wulff construction is closed only by (111) surface which is in agreement with experimental data. Cu dopping was modeled by exchanging two neighboring Ce atoms with Cu ions and creating 0,1 or 2 oxygen vacancies (Fig.l)
Figure 2. Catalytic activity of CuO/CeO2 samples (5 mol. %) in A) dry B) wet conditions. Samples prepared by: a - impregation, b - coprecipitation followed by impregnation, c - coprecipitation.
102

NOEA201I
Zakopane 4-7 September 2011
Catalytic tests showed that the CuOx/CeO2 samples obtained by impregnation were distinctly more active (exhibited lower Tx temperatures) in N2O decomposition in comparison to those synthesized by coprecipitation. This effect was practically insensitive to the presence of water (Fig. 2). Corresponding Tso values were equal to 430 and 540 °C in dry atmosphere and was shifted up to 500 and 600 °C in the atmosphere containing 3 vol. % of H2O. On the other hand, basing on the analysis of EPR, suggesting predominance of isolated copper species in the case of impregnated samples, it can be inferred that monomeric copper species are much more efficient as the active sites in N2O decomposition in comparison to dimeric copper centers.
Observed effect can be even more surprising if we take into account, that the determined from EPR spectra average Cu2+-Cu2+ distance in ionic dimers, equal to ca. 2.42 A, fits relatively well to the N-0 distance (ca. 2.55 A) in the bent N2O molecule (reactive mode). Adsorption of N2O on copper dimers should thus be preferrencial in comparison to that, when monomeric centers are engaged. Also DFT results suggested the lowest TS barrier (25.9 kcal/mol) for N2O adsorption on two vicinal copper centers exposed on CeO2 (111) surface.
Structural and morphological considerations led us to the conclusion that the confirmed relationships between structure of differently synthesized CuOx/CeO2 samples and their activity in deN2O reaction does not support the initial hypothesis ascribing a principal role in N2O decomposition to the coupled copper ions. Due to rather strong discrepancies in the structure and lattice parameters of CeO2 and CuO, as well as due to differences in sizes, electronegativities and charges of Ce4+ and Cu2+ ions, formation of a substitutional solid solution, in which vicinal copper centers could interact magnetically, giving rise to the characteristic fine structure in the EPR spectra, seems to be quite impossible. Most probably these entities are located in the subsurface interparticle layers, where copper ions segregate during thermal treatment of the CuOx/CeO2 samples. Such ions remain thus inaccessible for the reactants from the gas phase and even present, they cannot play a role of adsorption sites for N2O molecules.
The research was partially supported in the framework of the national grant No. NN 507 426 939 and carried out with the equipment purchased thanks to the financial support of the European Regional Development Fund in the framework of the Polish Innovation Economy Operational Program (contract no. POIG.02.0I.00-I2-023/08).
103

POSTER
SESSION

NOEA20II
Zakopane 4-7 September 2011
PS01
##### Dual role of surface nitrate species formed during NOX activation on supported oxometallic TMI clusters
##### A. ADAMSKI1, M. FIUK1, M. TARACH1, P. ZAPAŁA1, B. GIL1, Z. SOJKA1
1 Faculty of Chemistry, Jagiellonian University, 3 Ingardena St., PL 30-060 Cracow
It is well known from earlier studies on SCR NO, mechanism that adsorption of noxious nitrogen oxides (mainly NO and NO2) on supported clusters containing transition metal ions (TMI) may involve the formation of nitrite and nitrate species. Such forms can be stabilized over catalyst surface even up to 450-550 °C. Moreover, apperence of various nitrates can substantially lower the efficiency of NO, reduction by blocking catalytically active TMI sites. On the other hand, on basic oxides, under lean conditions, nitrates formation can be considered as a form of NO, storage. According to the generally accepted NSR mechanism, under rich conditions, nitrogen oxides can be subsequently released and efficiently reduced by hydrocarbons. Main problems can however be caused by the state of reducing agent and NO/NO2 ratio.
Even if the main steps of SCR NO, and NSR processes are alredy established, elucidation of the detailed redox mechanism accompanying NO, adsorption on supported oxometalic clusters, determination of experimental conditions favoring the formation of various surface entities and influencig their stability during oxidation and reduction cycles is still far from the final solution. There is a distinct gap in the state of our knowledge concerning the behavior of nitrites and nitrates formed during NO, activation under consecutive hydrocarbon/oxygen rich/lean conditions. The key point is related to the factors governing their reducibilily, which seems to be decisive for reversible character of nitrites/nitrates formation and thus for sucessful NO, removal. Present investigations on NO and NO2 adsorption performed on bare and TMI-modified zirconia and ceria may serve as model studies establishing a link between changes of structural properties induced by support oxide doping with TMIs and ability of a catalytic system to efficiently store and reduce NO, under reactive atmosphere of variable hydrocarbon/oxygen ratio.
EPR/IR results obtained after NO,, O2 and HC adsorption on a series of TMI-functionalized zirconia samples, containing nominally 0.2-5.0 mol. % of aliovalent additives (Mn2+/4+, Sm3+, V4+/5+ and Mo5+/6+), were confronted to those obtained for selected ceria- and Ce,Zr!.,O2-supported systems. TMI-doped samples were prepared by wet impregnation of the supports with aqueous solutions of the corresponding salts. All investigated samples calcined at 600°C/6h were structurally characterized by means of XRD and RS techniques. The gaseous reactants, were adsorbed at pressures of 2-20 Torr (non-equilibrium conditions) on the samples previously outgassed under vacuum at p < 10'5 Torr and activated at 350-400 °C for 0.5 h. Samples were contacted with gaseous adsorbates at LNT for 2 min and next exposed to room or elevated temperatures (Fig. 1).
107

NOEA2011
Zakopane 4-7 September 2011
Figure 1. Progress of NO activation during exposure of various TMI-modified ZrO2 (5 mol. %) samples to RT, monitored by EPR.
Adsorption of 10 Torr of NO over bare t-ZrO2 at LNT resulted in relatively weak chemisorptions of NO molecules accompanied by the formation of (Zr-NO)1 surface mononitrosyIs. as it can be inferred from the presence of the well resolved three line hyperfine structure visible in the EPR spectrum of N0/t-ZrO2. Observed signals were however not observed in the spectra of TMI-doped samples (5 mol. %), because of the overlapping of much more intense signals from the paramagnetic V4* (3d1), Mos+(4d‘), and Mn"+ ions.
Observed modes of NO adsorption distinctly reflected structural and redox properties of investigated TMI/r-ZrO2 samples. Three cases can be distinguished here: i) NO physisorption (5SmOx/ZrO2), ii) weak chemisorption without electron transfer (5MnOx/ZrO2) and iii) reductive adsorption - (5MoOx/ZrO2 and 5VOx/ZrO2). Low-temperature contact of the 5MoOx/ZrO2 and 5VOx/ZrO2 catalysts with 10 Ton of NO led to distinct changes in intensities of the EPR spectra without not accompanied by any new spectral features. Observed effects can be explained by the progressive reduction of V(V) and Mo(VI) centers by NO molecules via ligand to metal electron-transfer (LMET) according to the equations:
NO (2n1/2) + Mo6* (‘So) = ^-{Mo^-NOJ1
and NO (2n)c) + V5+('S0) = t]'-{ V4+-NO)‘
Parallel IR experiments confirmed that low-temperature (-120 °C) adsorption of 5-10 Ton of NO on 5Mo/Zr and 5V/Zr followed by exposure of these samples to RT, resulted in the formation of surface nitrates of bridging and chelating structure. NOX storage seems to be thus possible over these two TMVZtO2 catalysts. Reducibility of the observed nitrate species was subsequently verified in the reaction with selected hydrocarbons adsorbed at LNT or RT.
108

109
Figure 2. EPR spectra reflecting redox cycle for MoO/t-ZrO2 System
Concerted action of both oxidative (O2) and reducing agents (NO,, propene), strongly modifying redox state of TMI surface sites, can be in more detail illustrated with an example of MoO,/Zr02 samples (Fig. 2). Adsorption of NO led to partial reduction of the Mo(VI) to Mo(V). Subsequent propene adsorption was responsible for the reduction of the remaining Mo(VI) centers, as it can be inferred from increase of intensity of the previously observed signal. Reduction of surface molybdenum was however reversible. Consecutive O2 adsorption caused reoxidation of Mo sites. Simultaneously, the appearance of the new signal, ascribed to O2~ radicals, was observed. Introduction of the next portion of NO reacting with surface complexes resulted in nitrates formation, according to the eqation:
(Mo^-O/I1 +NO(2n)-> (Mo^-NO, )1.
If these nitrates were not reduced by the next portion of hydrocarbon, catalytic cycle cannot be closed. This step is vital also for NSR, where the target reduction product is nitrogen. The role of nitrates is thus crucial for catalyst performance and rejuvenation and therefore these aspect was particularly stressed in our studies.
The research was partially carried out with the equipment purchased thanks to the financial support of the European Regional Development Fund in the framework of the Polish Innovation Economy Operational Program (contract no. POIG.02.01.00-12-023/08).
NOEA2011
Zakopane 4-7 September 2011

NOEA 2011
Zakopane 4-7 September 2011
PS02
##### Comparison between Cs-Cu/ZrCh and Cs-Co/ZrCh catalysts for NOX reduction in the presence of toluene A. AISSAT13 D. COURCOT13, S. SIFFERT13*
1 Univ Lille Nord de France, F-59000 Lille, France
2 ULCO, UCE1V, F-59I40 Dunkerque, France
★Corresponding author: siffert@univ-littoral.fr, Tel.: +33-328658256 (S. Siffert)
Industries using combustion processes are often faced to nitrogen oxides (NOX) emissions problems [1,2], A catalytic treatment by hydrocarbons may be an advantageous route for the purification of such effluents [2]. The use of zirconia (ZrO2) and transition metal oxide phase are known to be powerful for NO, reduction [3] and also for hydrocarbons oxidation[4,5]. In some cases, alkali metals are known to be activity promoters for hydrocarbons oxidation as well as for NO; reduction [3], Cu and Co do not present the same behaviour towards NO; reduction. The effect of the alkali metal content (cesium) was studied on the physicochemical characteristics of ZrO2 and their catalytic properties in reduction of NO; by hydrocarbons.
ZrO2 support was prepared by a precipitation method. After drying at 115°C for 24 h, this solid was calcined under air flow (2 Lh1) at 300°C for 4 h. Cs-Cu/ZrO2 or Cs-Co/ZrO2 solids were then prepared by impregnation of CuCO3 nCu(OH)2 or CoCO3-nH2O salts respectively or co-impregnation of Cs2CO3 and the corresponding salt onto ZrO2. After drying, the samples were calcined under air flow at 600°C for 4 h. The as-obtained solids were denoted Csx-Cuy/ZrO2 or CS;-Coy/Zr02, where x (0.015 or 0.03) corresponds to Cs/Zr atomic ratios and y (0.1 or 0.2) Cu/Zr or Co/Zr atomic ratios. The catalysts were characterized by many techniques (BET surface areas, XRD, TG-DTA, TPR, FT1R). The reduction of NO; was carried out in a continuous flow reactor (900 ppm of NO/N2, 1000 ppm toluene and 10%O2/N2, lOOmLmin1). Before each activity test, the catalyst (lOOmg) was dried in air (2Lh', rCmin'1) at500°C for 4 h. The volume hourly space velocity (VHSV) was 105 000 h'1.
TPR results for Cs-Cu/ZrO2 catalysts showed that the CuO reduction signal is between 100 and 220°C with Cuoj/ZrO2 [6]. This temperature interval increases with increasing the Cs amount. Thus, the presence of Cs decreases Cu reducibility attributed to the copper-cesium interaction. For Cs-Co/ZrO2 catalysts (Fig. 1) several peaks are shown. Species responsible for peaks below 400°C would be small particles of Co3O4 on solid surface. However, for peaks beyond 500°C, the species would be attributed to zirconate cobalt. Results of NO; reduction by toluene (Table 1) demonstrate that the copper based copper solids are more active. However, in the absence of toluene (Fig. 2(A)), the cobalt based solids produce more of NO2 (which is reduced to N2 after toluene oxidation). Whereas, in the presence of toluene (Fig. 2(B)), the conversion of NO; is more important for Cu-based solids. This shows that produced NO2 is reduced to N2on Cs-Cu/ZrO2 solids and to NO on Cs-Co/ZrO2 ones. Ill
Ill

NOEA 2011
Zakopane 4-7 September 2011
Catalyst	M = Cu	M = Co
CsM3-Mo. JZrOi	36.5 (288°C)	17.2 (308°C)
Cs «. o/s-M,J/rO2	50.0 (390°C)	27.1 (389°C)
M„.,/Zr()2	46.4 (410°C)	32.8 (200-350°C)
Csm3-Mn2/'ZrO2	40.0 (277°C)	30.0 (282°C)
Cs0.0is-MO2/ZrO2	50.2 (276°C)	22.30 (304°C)
M02/ZrO2	47.5 (290°C)	25.8 (305°C)

112

NOEA 2011
Zakopane 4-7 September 2011
Figure 2. Outlet concentration of NO and NO2for Cs00is-Cu0i/ZrO2 and Cso.oi5-Coo.i/Zr02 catalysts:
(A) blank test without toluene, (11) test in the presence of toluene (a: NO2, b: NO and c: NOX).
The “Nord-Pas de Calais" Region, the “Syndicat Mixte de la Cote d’Opale” and European Union via Interreg IV "Redugaz project" are gratefully acknowledged for financial support.
111 T. Holma, A. Palmqvist, M. Skoglundh, E. Jobson, Appl. Catal. B 48 (2004) 95
1. V.l. Parvulescu, P. Grange, B. Delmon, Catal. Today 46 (1998) 233
2. A. Bueno-I.opez, J.M. Soriano-Mora, A. Garcia-Garcia, Catal. Commun. 7 (2006) 678
[4| 1). Pietrogiacomi, I). Sannino, S. Tuti, P. Ciambelli, V. Indovina, M. Occhiuzzi, F. Pepe, Appl. Catal. B 21 (1999) 141
1. M. Haneda, Y. Kintaichi, M. Inaba, H. Hamada, Catal. Today 42 (1998) 127
2. A. Aissat, D. Courcot, R. Cousin, S. Siffert, Catalysis Today DOI: 10.1016/j.cattod.2011.01.033 (2011)
113

NOEA20I1
Zakopane 4-7 September 2011
PS03
##### On the influence of exhaust gas composition for the selective reduction of NOX over Fe/ZSM-5 catalyst
##### D, ADOUANE1, J. STARCK1, P. Da COSTA1, X. JEANDEL2
1 Universite Pierre et Marie Curie (Paris VI),
Laboratoire de Reactivite de Surface - CNRS UMR 7609,
4 Place Jussieu, 75252 Paris 05, France; e-mail: patrick.da_costa@upmc.fr
2 Technocentre Renault, I avenue du Golf, 78288 Guyancourt Cedex
Nitrogen oxides (NO,) which are mixtures of NO and NO2 are produced by Diesel combustion and industrial processes, and contribute to different atmospheric pollution phenomena such as ozone depletion, smog and acid rains [ I ].
In recent years, great efforts have been shown by the car manufacturer in order to reduce the ecological impact of their vehicles by developing different technologies to limit emission of such air pollutants. One of the most efficient technologies is the so called NH3-SCR (selective catalytic reduction of oxides with ammonia as a reducing agent).
Several reactions occur over SCR catalysts during the reduction of NO, with NH3. The main reaction of SCR with ammonia which is well known as “standard SCR reaction” is [2-3]:
4NH3 +4NO + O2 —> 4N2+6H2O	(1)
The reaction with equimolar amounts of NO and NO2“fast-SCR” reaction is much faster than the main reaction (I):
4NH3 + 2NO + 2NO2 -r 4N2 +6H2O	(2)
These theoretical reactions must be taken in account without omitting that real conditions we meet in the exhaust gas are very complex. Gas exhaust includes, among others, water, carbon monoxide and unburned hydrocarbons. Very active SCR catalysts have been reported in the literature but the problem of deactivation under high temperatures and water [4-5] or poisoning by hydrocarbon coking [6-7] still remains unsolved in most cases. To meet the durability requirement of DeNO, catalysts, an improved understanding of the impact of chemical deactivation on catalyst activity for this application is needed. The aim of this work is to study the influence of the exhaust gas composition, such as the presence or the lack of water and hydrocarbon, on the SCR catalysts efficiency. The effect of NH3/NO, ratio on the NO, reduction was also investigated. Catalytic tests were carried out on active phase and monolith (carrots).
Commercial SCR honeycomb monolith catalyst consisted on Fe-ZSM5 coated on a cordierite monolith. The monolith was crushed in order to evaluate metal contents by elementary analysis. The catalyst was characterized by X-ray diffraction (XRD) and Transmission Electron Microscopy (TEM). Before runs and characterization, the monolith was calcined in industrial air at 500°C for 2 h, using a heating rate of 10°C min-1
The active phase was extruded and two types of experiments were performed:
1. On active phase;
2. On monolith.
Tab.l. Experimental conditions
	GSHV	Total flow	Catalyst volume
Active phase	90 000 (h-1)	250 (cc/min)	0.17 (cm3)
Monolith	90 000(h-l)	10 L/min	6.67 (cm3)

115

NOEA2011
Zakopane 4-7 September 2011
The different characterizations showed that iron is essentially present under oxidised form (Fc2O3 and a part of Fe3O4) and located outside and on the border of zeolithe particles. We can-not exclude the presence of cationic iron in the zeolithe channels.
Water effect was investigated on this commercial catalyst. An inhibitor effect of water only for temperatures higher than 220°C was observed. This phenomenon could be explained by a better oxidative capacity of ammonia in the absence of water and an adsorption competition between water and ammonia.
The effect of hydrocarbons on NOx conversion was also investigated. Catalytic tesLs were performed over washcoat and monolith in the presence of propene, decane and toluene as a representative mixture of exhaust gas. The presence of decane in the feed inhibits NOX conversion and leads to a coke deposit formation [8]. The same phenomenon was observed on monolith with toluene. The presence of propene leads to a slightly loss of performance (about a few percents) at low temperature. The influence of NH3/NOX ratio on NOX conversion has been studied. The results confirm the impact of NH^NO,, ratio on NOX conversion. The NH^O, ratio = 1.2 leads to a higher conversion compared to NH3/NOX ratio = 1 or 0.8 on both active phase and monolith.
[ 1 ] S. Roy, M.S. Hegde, G. Madras, Appl. Enr. 86 (2009) 2297
1. M. Devadas, O. Kro'cher, M. Elsener, A. Wokaun, N. Sóger, M. Pfeifer, Y. Demel, L. Mussmann, Appl. Catal. B 67 (2006) 187
2. M. Koebel, M. Elsener, M. Kleemann, Catal. Today 59 (2000) 335
3. J. N. Armor, Catal. Today 26 (1995) 147
4. L. Gutierrez, M. A. Ulla, E. A. Lombardo, A. Kovacs, F. Lónyi, J. Valyon, Appl. Catal. A 292 (2005) 154
5. S. Isarangura, N. Mongkolsiri, P. Praserthdam and P.L. Silveston, Appl. Catal. B 43 (2003) I
6. C. He, Y. Wanga, Y. Cheng, C. K. Lambert, R. T. Yang, Appl. Catal. A 368 (2009) 121
7. V. Sanchez-Escribano, T. Montanari, G. Busca, Appl. Catal. B 58 (2005) 19
116

NOEA201I
Zakopane 4-7 September 2011
PS04
##### DRIFTS-MS studies of NO reduction and NH3 oxidation over V-O-V catalyst
##### B. AZAMBRE1, J. BANAŚ2, M. NAJBAR2
Laboratoire de Chimie et Methodologies pour I’Environnement,
Universite de Metz, Rue Victor Demange, 57500 Saint Avoid, France
2 Faculty of Chemistry, Jagiellonian University, 3 Ingardena St., 30-060 Krakow, Poland,
e-mail: mnajbar@ chemia, uj.edu.pl
The anatase supported V-O-W catalysts are commonly used for selective NOK reduction (SCR) to nitrogen by ammonia [I]. Vanadia species are thought to be active in this reaction [1-3], Ammonia adsorption on acidic OH groups, formed as a result of the dissociative water adsorption is most frequently considered as the first step of this process [2,3]. However, coordinative ammonia adsorption is also considered as a first step of SCR [1]. Miyamoto et al. [2] and Topspe et al. [3] have assumed that SCR including ammonium ion formation goes on the basal (001) V2O5 surface [4]. However, Gąsior at al. [5] have revealed its the highest rale on the side faces of vanadia crystallites. Moreover, Anderson [6] has shown that dissociative water adsorption resulting in OH groups formation does not occur on (001)V205 face but it proceeds easily on some side crystallite surfaces. Broclawik et al. [7] have demonstrated, by DFT calculations, that the water dissociation cannot proceeds on (001)V205 surface. According to Yin DFT results [8], water adsorbs on vanadyl oxygen of (001)V205 surface by hydrogen bonding.
On the other hand, the (001) V2O5 monolayer depleted of vanadyl oxygen and/or vanadium in the interstitial position of W-0 or Mo-0 structures shows some activity in a direct NO decomposition to nitrogen and oxygen [9-12] al temperatures 150-200°C. At higher temperatures the dissociative oxygen adsorption, resulting in recovery of the vanadyl oxygen at the surface retards NO decomposition. Thus, the consumption of vanadyl oxygen in ammonia oxidation should facilitate coordinative ammonia adsorption as well as NO decomposition. The structure of the vanadia species on the surface of titania supported vanadia-based catalysts strongly depends on their thermal pre-treatmenl [1-3, 9-14]. The (001)V205 monolayer species being in equilibrium with vanadium in the surface interstitial positions of the V-W oxide bronze are formed during the calcination of the precursor of the catalyst at 460°C [14]. However, calcination at temperatures equal or higher than 520°C [13] causes the formation of the V2O5 nanocryslallites crystallites besides monolayer and interstitial vanadium atoms on the catalyst surface.
The first aim of this paper was to find the most active places for coordinative and cationic ammonia adsorption on the rutile supported V-O-W catalyst exposing interstitial vanadium atoms as well as monolayer and crystalline vanadia species.
The second aim was to determine the activity of both the ammonia ad-species in the interaction with gaseous nitric oxide at the lowest possible temperature and to check possibility of the direct NO decomposition al this lemperalure on the surface interstitial vanadium atoms or the reduced vanadia monolayer species.
The active sites for coordinative and cationic ammonia adsorption on the V-O-W catalyst exposing both nano crystalline and vanadia species and surface interstitial vanadium atoms in V-W oxide bronze were determined and their activity in NO reduction was estimated.
The NHrTPD at a 30-410°C range was followed by DRIFTS-MS. After cooling to 150° C NO reduction by ammonia ad-species was investigated.
Coordinative ammonia adsorption on main (001) surfaces of vanadia nanocrystallites and ammonium ions formation on OH groups on their side surfaces was observed. The ammonium oxidation by molecular oxygen above 230°C and lack of similar oxidation of coordinative ammonia up to 320°C was revealed.
117

NOEA2011
Zakopane 4-7 September 2011
On the contrary, coordinative ammonia species showed higher activity in NO reduction at 150 °C than ammonium ions did. The observed differences in the activity of both the ammonia ad-specics in O2 and NO reduction were ascribed to the differences in mechanisms of (hose reactions.
A direct NO decomposition was found to proceed on vanadium atoms in surface interstitial positions of V-W oxide bronze.
[ 1 ] P. Forzatti, Appl. Catal. A 222 (2001) 221
1. A. Miyamoto, K. Kobayashi, M. Inomata, Y. Murakami; J. Phys. Chem. 86 (1982) 2945
2. (a) N. Y. Topspe; Science 265 (1994) 1217; (b) N. Y. Topspe, J. H. Dumesic, H. Topspe, J. Catal. 151 (1995) 226; (c) N. Y. Topspe, J. H. Dumesic, H. Topspe, J. Catal. 151 (1995) 241
3. ASTM Card 9-387, Nat. Bur. Standards Circ. 539 (1958) 66-67
4. M. Gąsior, J. Haber, T. Machej and T. Czeppe, J. Mol. Catal. 43 (1988) 359
5. A. Andersson, J. Solid State Chem. 42 (1982) 263
6. E. Brocławik, A.Góra, M. Najbar; J. Mol. Catal. A 166 (2001) 31
7. X. Yin, A. Fahmi, H. Han, A. Endou, S. Salai Cheettu Ammal, M. Kubo, K. Teraishi, A. Miyamoto, J.Phys.Chem.B 103(1999) 3218
8. M. Najbar, A. Białas, J. Camra, B. Borzęcka-Prokop, Proc. 1st World Congress on Environmental Catalysis, Societa’ Chimica Italiana, Roma, 1995, p. 283-286
9. M. Najbar, J. Banaś, J. Korchowiec, A. Białas, Catal. Today 73 (2002) 249
10. J. Banaś, V.Tomaśić,A. Wesełucha-Birczyńska, M. Najbar,Catal.Today 119(2007) 199
11. J. Banaś, A. Wesełucha-Birczyńska, J.Camra, B. Borzęcka-Prokop, M. Najbar, Pol. J. Environ. Stud. 15 6A(2006)
12. A. Białas, B. Borzęcka-Prokop, A. Wesełucha-Birczyńska, J. Camra, M. Najbar, Catal. Today 119 (2007) 194
13. M. Najbar, A. Góra, A. Białas, A. Wesełucha-Birczyńska, Solid State Ionics 141-142 (2001)499
118

NOEA2011
Zakopane 4-7 September 2011
PS05
##### SEM -EDS studies of transition metal catalysts for NO decomposition
##### E. BIELAŃSKA1, M. ZIMOWSKA1,1. NAZARCZUK2, M. KOZICKI2,
##### M. NAJBAR2
Jerzy Haber Institute of Catalysis and Surface Chemistry,
Polish Academy of Sciences,8 Niezapominajek St., 30-329 Krakow, Poland
Faculty of Chemistry, Jagiellonian University, 3 Ingardena St., 30-060 Krakow, Poland
DeNO, is the most important aspect of environmental catalysis. NO interaction with the human respiratory system becomes dangerous at concentrations higher than 40 ppm and results in suffocation at a concentration higher than 500ppm. Therefore abatement of NO emission is one of the is a great challenge for the environmentalists. The selective catalytic NO reduction by ammonia to dinitrogen and water is at present commonly used for NO emission abatement from stationary sources.
There is a big effort to find a catalysts for a direct NO decomposition or for a reduction of NO by a reducer cheaper, not corrosive and more friendly for environment than ammonia.
It was noticed recently in our laboratory that oxide Fe-Cr-Ni system, formed on the acid-resistant austenitic steel supports during thermal cycles composed of termo-programed heating of the support followed by annealing at the final temperature shows high activity in direct NO decomposition as well as in NO reduction by carbon present in the off gases of power plants.
Physico-chemical characterization of Fe-Cr-Ni oxides was performed using oxide samples striped from the steel support.
X-ray powder diffraction and selected area electron diffraction were used to determine phases present in oxide Fe-Cr-Ni catalyst. The chemical composition of its surface nanolayers was determined by X-ray photoelectron spectroscopy.
Scanning electron microscopy (SEM) with X-ray energy dispersive spectroscopy (EDS) allowed to determine chemical composition of particular particles from the surface microlayers of the catalyst and to localize carbon particles in the dust. This paper presents the results obtained by SEM-EDS methods.
The measurements were done using high resolution field emission Scanning Electron Microscope JEOL JSM-7500F with INCA Oxford Instrument EDS system.
In Fig. 1 a BSE-COMPO image (a) of a typical area of the sample composed of the dust mixed with Fe-Cr-Ni oxide catalyst (dust:catalyst weight ratio equal to 4) - grown on the surface of the tube made of an acid-resistant austenitic steel 1H18N9T/1.45 41 in the course of several thermal cycles is presented. The cycles were composed of a thermo-programmed heating in air up to 840°C with the rate of 4°/min followed by annealing at 840°C for 4 h.
Figures l(b-e) contain characteristic x-ray maps of C, Fe, Cr and Ni in the surface micro-layers of that Fe-Cr-Ni oxide catalyst. The semi-quantitative chemical analysis in the micro-layer of the presented area (a) of the sample reveals the presence of:
34at.% C, 26.6at.% Si, 16.4at.% Al, 11,4at% Fe, 3at% Ca, 2.7at.% K, 1.9 at.% Mg, 1.5at.% Cr, 1.4 at.% Na and 0.8 at.% Ni (the sum of carbon, silicon and metals was taken as a 100%)
Comparison of the Fe, Cr and Ni distributions in the particles of the catalyst (clear ones in the down part of Fig. la) allows to reveal the presence of the iron oxide almost free of Ni and Cr ( e.g. the biggest light particle in the left bottom part of figures ) as well as mixed Fe- Cr -Ni oxides with low content of Cr and high of Fe and Ni (e.g. three light particles in the right bottom parts of Figs a, c, d and e) or relatively high content of Cr as well as of Ni and low content of Fe (e.g. small particles close to a center of images). This results are in a good agreement with those obtained by diffraction methods and allow for their better understanding.
Comparison of the COMPO image with C mapping allows to notice the presence of the shadow from the carbon particles on a inorganic part of the dust. The carbon particles positions has fundamental role in discussion of the mechanism of NO reduction by carbon.
119

NOEA 2011
Zakopane 4-7 September 2011
Figure I . BSE-COMPO-image (a), and x-ray mapping of C (b). Cr (c), Fe (d) and Ni (e) of the mixture of the Fe-Cr-Ni oxides (formed on the surface of the tube from acid-resistant austenitic steel IH 18Ni9T/l .4541 in the course of several thermal cycles composed of thermo-programed heating, 4" C / min, followed by annealing at 84ff'C in air) and the dust collected behind the electro-filters of the biomass-coal power plant (dust: oxides weight ratio equal to 4)
Publication co-financed by the European Regional Development bund under the Innovate Economy Operational Programme 2007-2013, POIG.01.01.02-12-112/09 project.
120

NOEA 20II
Zakopane 4-7 September 2011
PS06
##### XPS studies of NI-Cr-Fe oxide catalysts for NO decomposition
##### J. CAMRA1, J. DUTKIEWICZ1, M. KOZICKI1, M. NAJBAR*
1 Faculty of Chemistry, Jagiellonian University, 3 Ingardena St., 30-060 Krakow, Poland,
Ni-Cr-Fe mixed oxides forming on the surface of austenitic acid-resistant steel supports (tubes, sheets of foil or monoliths) in the course thermal treatments in oxygen containing atmosphere were found to be active in a direct NO decomposition.
a- F^Oj and spinal phase with lattice parameters close to those of NiFe2O4 were revealed in Ni-Cr-Fe oxide layers. However, the content of both phases and their exact chemical compositions were found to depend on: i/ a sort of the austenitic acid-resistant steel, ii/a foil thickness, iii /a rate of heating, iv/ an annealing temperature, v/ an oxygen content in the gas phase as well as vi/ a number of the thermal cycles.
The activity in direct NO decomposition was also found to depend on the conditions of thermal treatment.
To find correlation between the Ni-Cr-Fe oxide catalyst activity in the direct NO decomposition to nitrogen and average chemical composition of the surface nanolayers, the XPS measurements were performed for the most active catalysts.
In a Table below the XPS results for the Ni-Cr-Fe oxide catalyst formed on the surface of austenitic acid-resistant 1HI8N9T/ 1.4145 steel tube (wall thickness ca 1mm) in the course of a few thermal cycles, composed of the heating with the rate of 4K/min to 650°C and next annealing at this temperature for 4h, are presented.
The areas of Cr 2p3/2 and Ni 2p3/2 and Fe 2p3/2 peaks were used to determine cation contents in the catalyst surface nanolayers. The deconvolution of the distinctly asymmetric Fe 2p3/2 peak allowed to determine separately the contents of Fe3+ and Fe2+ cations.
Cations	Fe 2p’+	Fe 2p2+	Cr2p3+	Ni 2p2+
BE [eV]	711.1	709.4	576.5	854.2
at. [%]	22.6	39.6	27.8	10.0

Comparison of the contents of Fe, Cr and Ni in the surface nanolayers with those in microlayers (Fe - 83 at.%, Cr - 1 lat.% and Ni-7at.%) reveals a strong surface segregation of Cr and weaker of Ni during austenitic acid-resistant 1H18N9T/ 1.4145 steel oxidation.
Publication co-financed by the European Regional Development Fund under the Innovate Economy Operational Programme 2007-2013, POIG.0I.0I.02-12-1I2/09 project.
121

NOEA20I1
Zakopane 4-7 September 2011
PS07
##### Acid-activated vermiculites as catalysts of the DeNOx process
##### L. CHMIELARZ1, M. WOJCIECHOWSKA1, M. RUTKOWSKA1, A. WĘGRZYN1, A. ADAMSKI1, B. DUDEK1, R. DZIEMBAJ1, A. MATUSIEWICZ2, M. MICHALIK3
1. Faculty of Chemistry, Jagiellonian University, 3 Ingardena St., 30-060 Krakow, Poland
2. The Institute of Ceramics and Building Materials, Glass and Building Materials Division,
   Cementowa 8, 31-983 Kraków, Poland
3. Institute of Geological Sciences, Jagiellonian University,
   Oleandry 2a, 30-063 Kraków, Poland
Clay minerals arc very attractive materials serving for many various applications including catalysis and adsorption. There is a large group of clay minerals containing significant amount of transition metal cations, which are catalytically active in various reactions. Iron is a typical component of vermiculites, however iron ions are located mainly in the octahedral sheets of clay and therefore are not accessible for reading molecules during catalytic processes. A large number of papers devoted to acid-activation of clay minerals [e.g. 1 ] reported that this process leads to partial or complete leaching of cations (including iron ions) from the octahedral sheets of vermiculite. Acid-activation increases the specific surface area and porosity, while part of iron ions removed from the octahedral sheets is deposited on the particle surface. Therefore, such easy and cheap modification of clay minerals may result in their functionalization for catalytic processes in which iron plays an essencial role. Iron is known to be catalytically active in the process of selective catalytic reduction of nitrogen oxides with ammonia (SCR NOX) [e.g. 2], Our previous studies have show significant catalytic activation of vermiculites and phlogophiles modified with nitrous acid [3J. Therefore, the present studies were extended for the activation of vermiculite with other mineral acids. The goal was to establish the link between conditions of leaching and catalytic activity.
Vermiculite (S&B Industrial Minerals GmbH) was dispersed in the 0.8 M solution of HNO3 (or HCI or H2SO4) with a ratio of clay mineral mass to nitric acid solution of I g/10 cm3 and stirred at 95 °C for 2, 8 or 24 h. Then, the samples were separated by filtration, washed with distillated water, dried at I2O°C for 12 h and calcined at 600°C for 5 h.
The clay samples were characterized with respect to chemical composition (XRF), structure (XRD, FT-IR, UV-vis-DRS, EPR), texture BET, morphology (SEM) and surface acidity (NH3-TPD).
The catalytic experiments (SCR NOX process) were performed in a fixed-bed flow microreactor system with a continuous analysis of reaction products (QMS). The following composition of the gas mixture was used: [NO|=[NH3|=0.25%, [O2|=2.5%. Helium was used as a balancing gas at a total flow rate of 40 ml/min.
Acid-activation of vermiculite resulted in a partial leaching of Al3+, Mg2+ and Fe3+ ions from the octahedral sheets. As revealed by spectroscopic methods, a part of the components leached was deposited on the particles surface. Acid-activation significantly increased the specific surface area (from 8 m2/g to about 280 m2/g) and pore volume (from 0.02 cm3/g to about 0.25 cm3/g) but decreased the surface acidity.
Acid-activation of vermiculite increased their catalytic activity in the SCR NOx process (Fig 1), however its efficiency strongly depended on the type of used acid as well as duration of the acid-activation process. Wet chemistry processes accompanying the leaching of iron ions are quite complex and can determine both the status and speciation of iron species deposited on catalysts surface, resulting in differences of catalytic activity. The highest NO conversion with a relatively high conversion to nitrogen was reached for vermiculite activated with nitric acid. The progress of the SCR NOx process was only slightly limited by the side reactions of direct ammonia oxidation at temperatures above 5OO-55O°C. Therefore, acid-activation of vermiculites seems to be a very effective and cheap method for the obtaining of the catalysts for the high-temperature SCR NOx process.
123

NOE A 2011
Zakopane 4-7 September 2011
124

NOEA 2011
Zakopane 4-7 September 2011
125

NOEA 2011
Zakopane 4-7 September 2011
Figure /. Results of SCR NOx tests for vermiculite activated with nitric acid (A), sulphuric acid (B) and hydrochloric acid (C).
Authors acknowledge the Polish Ministry of Science for financial support in the frame of project N N507 426939 and S&B Industrial Minerals GmbH for montmorillonite supplying.
M.R. acknowledges the financial support from the International PhD Projects Programme “MPD chemia UJ" operated within the Foundation for Polish Science MPD Programme co-Jinanced by the EU European Regional Development Fund.
|l| P. Komadel, J. Madejova, in: F. Bergaya, B. K. G. Theng, G. Lagaly (Eds.), Handbook of Clay Science, Elsevier, Amsterdam, 2006, 263
1. L. Chmielarz, P. Kuśtrowski, Z. Piwowarska. B. Dudek, B. Gil, M. Michalik, Appl. Catal. B 88 (2009)331
2. L. Chmielarz, A. Kowalczyk, M. Michalik. B. Dudek, Z. Piwowarska, A. Matusiewicz, Appl. Clay Sci. 49 (2010) 156
126

NOEA2011
Zakopane 4-7 September 2011
PS08
##### Is Hydrogen the main NOX reducing agent at low temperature for a CNG 3-way catalysts?
##### M. ADAMOWSKA1, S. CAPELA2, M. SALAUN1, L. GAGNEPAIN3, P. Da COSTA1
1. UPMC Paris 6, Institut Jean Le Rond d’Alembert, UMR 7190,
2. place de la gare de ceinture, 78210 Saint-Cyr L’Ecole, France
2 GDF SUEZ, Direction de la Recherche et de I’Innovation, 361 Av. du President Wilson,
B.P. 33, La Plaine Saint-Denis Cedex, France,*sandra.capela@ gdfsuez.com
ADEME - Departement Transports et Mobilite,
500 route des Lucioles, 06560 Valbonne, France
Rigorously regulated automotive exhaust gas emissions according to standards as Euro 4 (in effect since January 1,2005) or Euro 5 (September 1,2009), demands the employment of efficient strategies for emission reduction. Natural Gas (NG), primarily composed by methane, is regarded as one of the most promising alternative fuels: natural gas engines produce lower PM than diesel and for NG combustion lower combustion temperatures are required which leads to a decrease of NOx emissions [I]. For CNG 3-way catalysts, total NO conversion can be reached by its reaction with methane at high temperature (T>300°C) [2]. However, CO and H2 are also known by their reducing properties [2,3,4] specially at relatively low temperature. The main global reduction reactions that take place in CNG conditions are:
NO + H2 ='/2N2 + H2O	(1)
NO + CO = ‘/2N2 + CO2	(2)
4NO + CH4 = 2N2 + CO2 + 2H2O	(3)
NOx abatement at low temperature has been deeply studied in the automobile industry and, in the case of CNG vehicles, hydrogen (and CO) appears as one of the promising reducing agent capable to react with NO atT<300°C |2,5,6,7], Normally platinum is considered as the most active noble metal for such reactions: NO-CO and specially NO-H2.
The aim of this work is to study the effect on the NOx treatment at low temperature by changing the NO/H2 ratio of simulated exhaust gas composition in synthetic gas bench scale on monolithic reactor.
The catalytic tests were performed on a commercial CNG catalyst in a monolith form which dimensions are 1 inch diameter x 1,9 inches length. This catalytic converter corresponds to conventional active phases coaled on a ceramic honeycomb monolith.
The metal loading of the catalyst was obtained by ICP (Induced Coupled Plasma) elemental analysis. Catalytic tests were performed on a Synthetic Gas Bench (SGB) which reaction mixture was defined as follows: 0.25% NO, 0,17% CH4, 0,48% of O2, 9,25% CO2, 0,47% CO, 0,34% H2 and 18% H2O. This conditions lead to richness of 1,005 representative of a sparck. The GHSV was fixed at 40000h '. Different runs where performed in varying the CO/H2 ratio from 0 to 1,5.
Catalyst Characterisation
ICP analysis showed that the commercial catalyst presented the following composition:
Table 1: Noble metals loading (%wt.)
Pd	Rh	Pt	Ce
1,40+0,05	0,05±0,02	0,09±0,03	3,07+0,30

127

NOEA2011
Zakopane 4-7 September 2011
This catalyst is high loaded on palladium and it was detected a residual loading of Rh and Pt. From TEM and XPS, one can conclude that palladium is only present in oxidized form (PdO or Pd +11).
Catalytic tests
In Figure 1, we presented the pollutants evolution with temperature. Both Light off plots present a similar pollutants evolution, especially from 300°C: NO and methane are completely converted in N2 and CO2, respectively, according to the global reaction 3 mentioned above.
Figure 1. CO, NOx and CH4 profile during temperature programmed reaction with a) 1^00=0,5 and b) 1^00=1,5
Crucial differences observed among these two tests appear between 100 and 200°C. The increase of the hydrogen amount in the exhaust gas leads to an increase of NO conversion at low temperature: using a ration H2/CO=1,5 (Fig. lb), it is observed a total NO conversion at 160°C, assuring the role of H2 as the main reducing agent in this temperature domain.
128

NOEA 20II
Zakopane 4-7 September 2011
Comparing the results obtained during the catalytic tests and the ICP results, the presence of palladium seems to have a major importance on the NO-H2 reaction.
Recent studies have been developed concerning the NOx treatment at low temperature. Hydrogen and CO are well known as the main reducing agents acting at this temperature range, but with this catalyst, H2 seems to be the most interesting one. However, it remains very important to check the selectivity of the NO-H2 reaction in N2.
This work was carried out in the framework of ANR PREDIT “CARAVELLE". M. Salaun acknowledges ADEMEfor phD Grant.
11] K. S. Varde, G. M. M. Asar, SAE Paper 2001-28-0023 2001
1. M. Salaun, A. Koaukou, S. Da Costa, P. Da Costa, Appl. Catal. B doi: 10.1016/j.apcat.2008.10.026
2. E Dhainaut, S. Pietrzyk, P. Granger, Catal. Today 119 (2007) 94
3. R. D. Clayton, M. P. Harold, V. Balakotaiah, Appl. Catal. B 81 (2008) 161

NOEA20II
Zakopane 4-7 September 2011
PS09
##### Influence of the ion exchanged metal (Cu, Co, Ni and Mn) on the selective catalytic reduction of NO over mordenite and ferierite
##### W. ĆWIKŁA-BUNDYRA1
1 Department of Environmental Chemistry, University of Marie Curie-Sktodowska,
Marie Curie-Sklodowska Sq., 20-031 Lublin, Poland,
e-mail: wieslawa.cwikla-bundyra@ poczta,umcs.lublin.pl
Nitrogen oxide is produced during fuel combustion at high temperature. It is considered to be the most toxic exhaust gases. While the requirements on the purity of exhaust gases were becoming more rigorous it turned out to be necessary to look for techniques reductions of NO in exhaust gases. Catalytic reduction with hydrocarbons is believed to be the most promising way to eliminate nitrogen oxide. The main advantage of the corresponding reaction is the use of gas mixture very similar to that found in exhausts. In this paper, transition group metals (Cu, Co, Ni and Mn)-loaded zeolite are examined for the selective catalytic reduction of NO by methane.
All catalysts were prepared by the ion exchange method described in the literature [1]. The content of pure metal introduced to the catalysts was measured with the XRF method.
Measurements of the rates of NO reduction were carried out in a gradient less reactor based on the one described in paper [2] in the temperature range 200-500° C. The reaction rate was calculated using the equation valid for a gradient less reactor. All kinetic experiments were carried out determining isothermally the relationship between the reaction rate of NO reduction and degree of NO conversion. The reaction products were analyzed chromatographically.
Table 1 lists, for all catalysts, ion exchanged metal content and the ion exchange level.
Table 1. Catalyst composition and main characteristics
Samples	Metal loading |wt %]	Ion exchange level / (%)	Mas ratio of Si/Al
Cu-l-30-MOR	1,92	53
Co-l-30-MOR	1,80	49
Ni-l-30-MOR	1,44	40	5,8
Mn-l-30-MOR	1,08	30
Cu-l-30-FER	2,82	66
Co-l-30-FER	2,36	55	7,8
Ni-l-30-FER	2,04	48
Mn-l-30-FER	1,99	46

131

NOEA2011
Zakopane 4-7 September 2011
Figure 1. The conversion of NO (mol%) in the presence of methane on pure Co-, Cu-mordenite
The reaction of reduction NO in inert atmosphere was followed by monitoring NO consumption, N2 production and selectivity to N2, as a function of time on stream in the temperature range 200-500°C. The catalytic results at different temperatures for the examined catalysts are shown in figure 1
132

NOEA2011
Zakopane 4-7 September 2011
Figure 2. The conversion of NO (mol%) in the presence of methane on pure Co-, Cu-ferrierite
Selective catalytic reduction of NO by methane was investigated on Cu, Co, Ni and Mn ion exchanged mordenite and ferierite in the presence of excess of oxygen. The catalytic activity showed for all the catalysts increased with increasing metal content reaching a maximum of NO conversion. NO conversion increased with the reaction temperature passing through a maximum, and then decreased at higher temperatures, due to the combustion of the hydrocarbon, which reduced the amount of reductant and become dominant at higher temperatures. NO TOF for all the catalysts here prepared was analyzed at 375-500°C. It was observed that this parameter decreased with the metal content and, regardless the type of zeolite and ion exchanged metal introduced in the catalysts, all the experimental points were correlated by an unique curve. The results presented have emphasized a significant point concerning the course reduction of nitrogen oxide by methane, that the reaction mechanism is determined by the catalyst used [3.4],
T. Yamamoto, A. Eiadua, S. Kim, T. Ohomori, J. Ing. Eng. Chem. 13 (2007)
133

NOEA 2011
Zakopane 4-7 September 2011
1. D. Nazimek, J. Ryczkowski, Ads. Sci.Technol., 17(1999)360
2. H. Hamada, Catal. Today 22 (1994) 21
3. A. Kubacka, J. Janas, B. Sulikowski, Appl. Catal. B 69 (2006) 43
134

NOEA2011
Zakopane 4-7 September 2011
PSIO
#### Structural studies and physicochemical properties of new molybdenum peroxocomplexes with nicotinic acid
#### A. DOBIJA1, W. NITEK1 2 3 3, W. ŁASOCHA1*2
1 Jerzy Haber Institute of Catalysis and Surface Chemistry PAS,
Niezapominajek 8, 30-239 Cracow, Poland
2 Faculty of Chemistry Jagiellonian University, Ingardena 3, 30-060 Cracow, Poland
Peroxocomplexes with transition metals are an interesting group of compounds important in the processes of catalytic oxidation of alcohols, sulfides [1], epoxidation etc. In general, molybdenum compounds are important substrates in catalysts syntheses, many of which are used in air cleaning processes [2], hydrodesulfurisation, propene selective oxidation, ammoxiation, accrolein oxidation, olefin metathesis and many others.
Four new molybdenum peroxocomplexes with nicotinic acid have been synthesized and characterized with the use of XRD, thermal decomposition, SEM and IR spectroscopy. Compound 1 NHCjFLCO^MoOfO^OFŁ) (see Fig. 1) crystallize in space group Pc, compound 2 2[C5H4NCO2(O[MoO(O2)2])] ■ 2NH4+ crystallize in triclinic crystal system in P-1; compound 3 2[C5H4NCO2(O[MoO(O2)2]}] • 2C6H6NO2 • 2H2O crystallize in space group P2/c; compound 4 NHC5H4CO2(MoO(O2)2OH2) crystallize in space group P4:22. Although, some complexes with nicotinic acid were already described in literature [3], according to published data they differ from those obtained in our laboratory. In addition, compounds described in the literature have not investigated by X-ray single crystal methods. After thermal decomposition of our peroxocompounds, nano-metric molybdenum trioxide is formed, which could also lead to significant practical and technological applications.
Figure 1. a) Asymmetric unit and b) unit cell packing of peroxomolybdenum complex 1. Cell parameters a=5.416(3), b=5.350(2), c=16.976(7)A, 0=106.23(3)
The research has been partly supported by the EU Human Capital Operation Program, Polish Project No. POKL.04.0101-00-434/08-00
[1]	J. Nasrin, M. S. Islam. J. of Appl.Sci. 7 (2007) 597
[2]	W. Łasocha, A. Rafalska-Łasocha, M. Grzywa, B. Gawel. Catal. Today 137 (2008) 504
[3]	C. Djordjevic, B. C. Puryear, N. Vuletic, C. J. Abelt, S. J. Sheffield. Inorg. Chem. 2 (1988) 2926
135

NOEA2011
Zakopane 4-7 September 2011
PS11
##### Effect of soot on NO decomposition in O2 and SO2 presence over Ni-Cr-Fe oxide catalysts
##### J, DUTKIEWICZ1, S. JANIGA1,1. NAZARCZUK1, M. KOZICKI1, P. KORNELAK1, M. NAJBAR1
1 Faculty of Chemistry, Jagiellonian University, 3 Ingardena St., 30-060 Krakow, Poland
The main ecological problem nowadays, linked to technological boom in advanced countries, is an emission of air pollutants.
Nitrogen oxides NOX arc the main air pollutants. They cause damage of a human respiratory system, acid rains, a stratospheric ozone destruction, a greenhouse effect, abatement of plant vegetation, building elevation destroying and metal corrosion.
Nitrogen oxides are formed mainly by forests fires, lightning, volcanoes’ explosions and soil bacteria.
The men activity linked to NOX emission is related to fossil fuel combustion (petrochemical industry, transport, energy production) and nitric acid obtainment. The main NOX component in flue gases of stationary emission sources is NO.
Recently the basic process for NOX control from stationary emission sources is SCR by NH3. This process is selective to N2 also in oxygen presence in the feed. V^-WO^anatase catalysts are commonly used in this process.
Unfortunately this process has also some drawbacks: ammonia belongs to very corrosive compounds and it is relatively expensive and poisoning; the catalysts undergo deactivation under the influence of As2O3 and SO2
Another way of NO emission abatement from the stationary sources of emission is its direct decomposition. The main advantage of this process is that it does not need any reducer, so does not generate other pollutants. Il is mostly investigated over noble metals and zeolites with incorporated cuprum or cobalt ions as well as on some mixed oxide of transition metals.
We have found recently that Ni-Cr-Fe mixed oxides formed during oxidation of the austenitic acid-resistant steel supports show high activity (CN0) in the direct NO decomposition and relatively high selectivity to N2 (SN2).
The direct NO decomposition over the Ni-Cr-Fe oxide catalysts was investigated al temperatures 150-500°C. A quartz tubular reactor with GC (Molecular Sieve 5A column and TCD detector) or quartz u-tube flow reactor with MS detector were used for catalytic tests. The contents of NO in reaction mixtures were equal to 2%, 1% and 200ppm and GHSV was close to 15000 h1. In most of the tests 5-7.4 %O2 was added to the reaction mixture. In several tests 200-16000 ppm SO2 was also introduced. In a few tests the catalyst was mixed with a dust collected behind the electro-filters of the biomass-coal power plant.
In a Fig. I the temperature dependences of the selectivity to N2 in direct NO decomposition on the Ni-Cr-Fe oxide catalyst (200mg) in the reaction mixtures containing: a) 2%NO/He; b) 2%NO and 5%O2/He; c) 2%NO and 1600ppmS02/He; d) 2%NO, 7,4%O2 and 200ppmS02/He (0.05g of the dust mixed with the 0.200g of the catalyst) are presented. The NO conversion in all the experiments is equal to 100%.
The selectivity to N2 increases in the course of the temperature increase. The highest selectivity to N2 (100%) is achieved for NO decomposition in 2%NO/He mixture at 250°C -350°C. The addition of oxygen to the reaction mixture causes some decrease of the selectivity to N2 (b). A much stronger decrease of the selectivity to N2 is caused by the addition of l600ppm SO2 (c). If NO decomposition in the feed consisting of 2%NO, 7,4%O2 and 200ppmS02 proceeds on the catalyst mixed with 50mg of the dust, collected behind the electro-filters, the selectivity to N2 is very low at 150-300°C, rapidly increases at 350°C and reaches ca. 90% at 400-500°C.
MS analysis of the products formed on that catalyst containing different amounts of the dust reveals that at 300°C oxygen oxidizes the carbon mostly to CO. Next carbon monoxide reduces NO mostly to N2.
137

NOEA 2011
Zakopane 4-7 September 2011
Figure 1. The selectivity to N2 in the direct NO decomposition on 200mg of the Ni-Cr-Fe oxide catalyst (a-c) or on the mixture of that catalyst with 0.05g of the dust (d) in the reaction mixtures containing: a) 2%NO/He; b) 2%NO and 5%O2/He; c) 2%NO and lóOOppmSOfHe;, d) 2%NO, 7,4%O2 and 200ppmS02/He; GHSV=15000 h1
Publication co-financed by the European Regional Development Fund under the Innovate Economy Operational Programme 2007-2013, POIG.Ol.01.02-12-112/09 project.
138

NOEA2011
Zakopane 4-7 September 2011
PS12
Surface, structural and morphological characterization
of nanocrystalline ceria-zirconia mixed oxides upon thermal aging
I. DOBROSZ-GÓMEZ1, M. A. GÓMEZ-GARCIA1, M. I. SZYNKOWSKA2,
I. KOCEMBA2, J. M. RYNKOWSKI2
1 G.I.A.N.T., Grupo de Investigation en Aplicadón de Nuevas Tecnologias,
Universidad National de Colombia, Sede Manizales, Colombia
2 Institute of General and Ecological Chemistry, Technical University of Łódź,
90-924 Łódź, Żeromskiego 116, Poland
Ceria and ceria-based materials (especially its substitutional solid solutions) have attracted much attention in recent years mainly due to their application as a crucial component of modem catalysts used for automotive emission control (TWCs). It is generally known that the incorporation of zirconium into the ceria lattice creates more defects, which can stabilize ceria against sintering, enhancing the thermal stability and the efficiency of the TWCs. In the theory, the catalytic activity is directly related to the chemical composition and the structure of the catalyst. Materials with nanocrystalline structure, characterized with high surface area and high porosity are desired for the practical applications, taking into consideration their potential kinetic advantages.
Several methods have been used for the synthesis of nanocrystalline CeO2-ZrO2 solid solutions, including co-precipitation, direct hydrothermal synthesis, sol-gel technique, polymerized complex method, the amorphous citrate process, gel combustion, evaporation induced self-asambley (EISA), hard-template method, etc. (1,2). The obtained materials differed in the surface area, crystallite size, crystalline structure, reducibility, etc., confirming that the preparation method can strongly affect the surface and structural properties of CeO2-ZrO2 oxides. Moreover, some of the obtained oxides contained chlorine ion which is commonly known as a poison of three-way catalyst. It should be also noted that some of these approaches are complicated and presents limitations, which are not suitable for large scale applications. On the other hand, some of them (e.g. sol-gel and citrate complexation) do not guarantee the homogeneity of the produced materials in all compositional range (3). Therefore, reliable synthetic routes for synthesis of Ce-Zr mixed oxides as nanoparticular powders in the wide compositional range and preferably via low-energy chemical steps arc required.
In this work, a variant of sol-gel technique known as sol-gel like method (4) was employed to obtain nanocrystallinc, homogenous in size dimension and morphology, Ce-Zr solid solutions in a wide compositional range. It should be noted that several papers have been reported the physico-chemical properties and catalytic performance of Ce-Zr mixed oxides. However, contradictory informations can be found in the literature, especially over “the best” Ce-Zr composition in the terms of the thermal stability and redox properties: either CeO2- or ZrO2 rich, or Ce^Zr 05O2 has been already indicated as the most effective compositions (5-7). Herein, we present the systematic characterization of the physico-chemical properties of fresh and thermally aged Ce^Zr,^ (0 < x < 1) mixed oxides. The relationship between the surface, structural and morphological properties of the Ce/Zr molar ratio upon thermal aging was studied by means of different techniques, such as TGA-MS, N2-BET, SEM-EDS, XRD. It was of particular interest to determine “the best composition” of CehxZrxO2 (0 < x < 1) mixed oxides upon thermal aging, considering also its catalytic performance. In this study, CO oxidation was used as test reaction.
Very homogeneous in size dimension and morphology, nanosized, Ce|.xZrxO2 (0 < x < 1) materials were synthesized by the sol-gel like method. The existence of a single cubic structure of CeO2 and both monoclinic and tetragonal ones of ZrO2 was confirmed. In the whole composition range, dissolution of ZrO2 into CcO2 lattice was observed, accompanied by the formation of a fluorite-type structure in the case of the 75/25 mixed oxide composition and tetragonal one for ZrO2 content > 50 mol %. The formation of single phase, homogenous solid solutions was confirmed. The extent of crystallite agglomeration was increasing gradually with ZrO2 substitution in Ce02-ZrO2 solid solution powders. Upon thermal aging, the
139

NOEA 2011
Zakopane 4-7 September 2011
crystalline phases of CerxZrxO2 (0 < x < 0.75) powders remain unchanged. Only for ZrO2, the transformation of t-ZrO2 into m-ZrO2 was observed. No phase segregation for Ce!.xZrxO2 mixed oxides into a CeO2-rich and ZrO2-rich mixture was detected, indicating the presence of compositionally homogenous solid solutions. A strong effect of the samples composition on their specific surface area (SBet) >s observed. The values of SBEr were decreases in the following order: CeO2 > CcojsZro^Ą > Ceo5Zr0502 > Ceo.25Zro7502 > ZrO2. Upon thermal aging, a lower decrease in the surface area of CeO2-ZrO2 mixed oxides compared to pure oxides is observed, confirming the preventing role of ZrO2 addition into CeO2 in the sample sintering. The strong effect of the oxide composition on the sintering of Ce|.xZrxO2 oxides is observed. The lowest sintering effect was detected in the case of the 75/25 mixed oxide composition. The specific activity of CeO2-ZrO2 mixed oxides in CO oxidation was found to be dependent on Ce/Zr molar ratio. The 75/25 solid solution composition shows the highest specific activity among the studied oxides. The significant effect of the average crystallite size on the oxide catalytic performance is observed. The lower the crystallites size the solid contains, the higher is the activity in CO oxidation. The influence of the presence of small agglomerates on the specific activity of Ce|.xZrxO2 oxides was detected. The higher amount of agglomerates the solid contains, the lower is the activity in CO oxidation. The incorporation of ZrO2 into CeO2 lattice enhances both ils resistance against sintering and its catalytic performance, especially as long as cubic symmetry of mixed oxides is maintained. Higher surface area, the presence of smaller particles and a lower amount of particles agglomerates generate a better catalytic performance of Ce|.xZrxO2. Those oxides exhibit a higher amount of crystal faces, edges, and comers, conventionally considered as active sites for the adsorption of reactants in comparison to the sintered powders.
[ 1 ] R.O. Fuentes, R.T. Baker, J. Phys. Chem. C 113 (2009) 914 and references therein
1. Ch. Li, X. Gu, Y. Wang, Y. Wang, Y. Wang, X. Liu, G. Lu, J. Rare Earths 27 (2009) 211 and references therein
2. M. Alifanti, B. Baps, N. Blangenois, J. Naud, P. Grange, B. Delmon, Chem. Mater. 15 (2003) 395
3. H. Provendier, C. Petit, J.-L. Schmitt, A. Kiennemann, C. Chaumont, J. Mat. Sci. 34 (1999) 4121
4. H. Vidal, J. Kaspar, M. Pijolat, G. Colon, S. Bernal, A.M. Cordon, V. Perrichon, F. Pally, Appl. Catal. B 27 (2000)49
5. A. Trovarelli, C. de Leitenburg, G. Dolcetti, Chemtech 27 (1997) 32
6. M. Fernandez Garcia, A. Martinez Arias, A. Iglesias Juez, C. Belver, A.B. Hungria, J.C. Conesa, J. Soria, J. Catal. 194(2000)385
140

NOEA 2011
Zakopane 4-7 September 2011
PS13
##### Nanostructured Co-Ce-O systems for catalytic decomposition of N2O
##### R. DZIEMBAJ1, M. M. ZAITZ1, M. RUTKOWSKA1, M. MOLENDA1,
##### L. CHMIELARZ1
1 Faculty of Chemistry, Jagiellonian University, 3 Ingardena St., 30-060 Krakow, Poland
Nitrous oxide (N2O) presents in air has come from both natural and antropogenic emission. The major sources of this emission are chemical industry (e.g. production of nitric acid, adypic acid, caprolactam, glyoxal), agricultural soil management, animal manure management, sewage treatment and combustion of fossil fuels. N2O is considered as a strong greenhouse gas with very high (near 300 times larger than an equal mass of CO2) global warming potential. Nitrous oxide is also known to take part in the catalytic destruction of the stratospheric ozone succeeding its photolytic oxidation to nitric oxide (NO). It is estimated its almoust linear increase of 0,26% N2O per year due to emission from the human-related sources!I]. One of the most promisful way of reduction of N2O emission is its catalytic decomposition to nitrogen and oxygen.
Two series of nanostructured materials were prepared using a modified reverse microemulsion method [2], The first series was composed of ceria nanograins doped with cobalt ions, while the other was based on cobalt spinel doped with cerium ions. The obtained precursors were subjected to thermal analysis (EGA-TGA/DTG/SDTA) in order to determine optimal calcination temperature. The crystal structure and phase characterization of the powders was determined from XRD measurements, supported with the scanning electron microscopy (SEM). Elemental analysis of the catalysts were performed using the optical emission spectroscopy with inductively coupled plasma (ICP-OES). Surface morphology, specific surface area and pores distribution were evaluated on the basis of the BET method.
141

NOEA 2011
Zakopane 4-7 September 2011
Figure / The catalytic decomposition of N2O on a) Ce/ xCoxO23 and b) cobalt spinels
All the ceria doped materials formed mono phase solid solutions, showing a fluorite-like structure. The second group of materials, cobalt spinel doped with cerium ions, formed core-shell type grains with distinctly separated two phases of the cobalt spinel covered with thin layer of ceria. All the materials (from both series) were tested as catalysts in N2O decomposition showing high activity hut those based on the cobalt spinels (binary phase grains) showed better catalytic performances in N2O decomposition. The differences in catalytic activity of these two series of the catalysts were discussed in relation to their crystal and electron structure.
Acknowledgement: This work was supported by Research Project Grant number N N209 099337, from the Polish Ministry of Science and Higher Education. The part of the measurements was carried out with the equipment purchased thanks to the financial support of the European Regional Development Fund in the framework of the Polish Innovation Economy Operational Program (contract no. PO1G.02.01.00- 12-023/08).
1. S. Surinder, Agriculture, Ecosystems & Environment, 136(2010) 1X9
2. R. Dziembaj, M. Molenda, L. Chmielarz, M. Drozdek, M. M. Zaitz, B. Dudek,
A. Rafalska-Łasocha, Z. Piwowarska, Catalysis Letters, 135 (2010) 68
142

NOEA201I
Zakopane 4-7 September 2011
PS14
##### Membrane reactor for ammonia decomposition - design guides M. A. GOMEZ-GARCIA1.1. DOBROSZ-GÓMEZ1, J. FONTALVO1,
##### J. M. RYNKOWSKI2
1 G.I.A.N.T., Grupo de Investigation en Aplicación de Nuevas Tecnologtas,
Universidad National de Colombia, Sede Manizales, Colombia
2 Institute of General and Ecological Chemistry, Technical University of Łódź,
90-924 Łódź, Żeromskiego 116, Poland
Air pollution, due to the use of fossil fuels for power generation, is one of the main environmental problems of the 21 st century society [1], For NOX emissions control from stationary sources, various alternatives are available today. Selective Catalytic Reduction (SCR) technology is a current large-scale commercial practice. The main chemical reaction for NOX SCR process is:
4M9+4NH2 + O2 <=> 4/V2 + 6H2O	(1)
In fact, the industrial control of NO removal in commercial units can be accomplished by injecting of the required amount of NH3 to the flue gases. Typically, in a SCR process, 1-1.5 m3 of catalyst is required for each megawatt of electric power generating capacity while providing more than 80% of NO removal [2], Characteristic operating temperatures are in the range 600 - 900 K, and gas space velocities (GHSV) are in the 2000 - 7000 h'1 (STP) range [3], Besides its known advantages, SCR technology has several important drawbacks. One of the most important is related with the ammonia slip. The more tightening environmental regulations obligate to improve the actual SCR technology while keeping its outstanding features. Ammonia removal by decomposition has been proposed in the literature by different authors [4]. Since the ammonia decomposition is thermodynamically limited, a membrane reactor appears as an alternative. However, in the literature, methodologies for the analysis and design of membrane reactors have been rarely addressed [5]. In this work, a systematic approach for the feasibility analysis of a membrane reactor for the ammonia decomposition is presented.
The equilibrium shift in a membrane reactor is accomplished. Pressure and sweep gas flow rate are included in the analysis (Figure 1). The effect of permeation rate, reaction rate, and selectivity on the exit conversion is also considered. Two dimensionless groups, Pe and Da, are employed to represent the relative magnitude of permeation rate and reaction rate to conversion, respectively. This allows constructing a design chart for the ammonia decomposition system (Figure 2). A mathematical model including conservation of mass in the tube and shell side of reactor is proposed. The proposed model was solved numerically and lhe effects of different parameters on the rector performance were investigated. The effects of pressure, temperature, flow rate (sweep ratio), membrane thickness and reactor diameter have been investigated in the present study. Increasing ammonia conversion was observed by raising the temperature, sweep ratio and reducing membrane thickness. When the pressure increases, the decomposition is gone toward completion but, at low pressure the ammonia conversion in the outset of reactor is higher than other pressures, but complete destruction of the ammonia cannot be achieved (Figure 3).
The proposed model can be used for design of an industrial catalytic membrane reactor for removal of ammonia from ammonia plant and reducing NOX emissions.
143

NOEA 2011
Zakopane 4-7 September 2011
144

NOE A 2011
Zakopane 4-7 September 2011
Figure 3. Conversion as a function of reactor length for different feed temperatures
1. K. Schnelle, in: C. Brown (Ed.), Air pollution control technology. CRC press; N. Y., 2002
2. A. Cybulski, in: J. Moulijn (Ed.), Structured Catalyst and reactors. Marcel Dekker, 1998
3. J. Beeckman, L. Hegedus, Ind. Eng. Chem. Res. 30 (1991) 969
4. M. R. Rahimpour, A. Asgari, J. Hazard. Mat. 153 (2008) 557
5. Y-S. Huang, E-U. Schliinder, K. Sundmacher, Cat. Today. 104 (2005) 360
145

NOEA2011
Zakopane 4-7 September 2011
PS15
##### IR studies of the coadsorption of CO and electron donor molecules on Cu+ sites in CuZSM-5 zeolite
##### K. GORA-MAREK1
1 Faculty of Chemistry, Jagiellonian University, 3 Ingardena St., 30-060 Krakow, Poland
Many studies have been devoted to the properties of the Cu+ sites in zeolite due to their catalytic activity in denox processes. It is well known that the exchangeable cations are modified by the framework oxygens as well as by the interaction with reagent molecules. The goal of the present study was to follow the ability of the Cu+ cations to activate the CO in the presence of the preadsorbed molecules of the different electron donor properties e.g. NH3, pyridine, and H2O.
The sorption of CO at room temperature in CuZSM-5 results in the formation of the Cu+(CO) monocarbonyls (the band at 2157 cm1) (Fig.l, spectrum a), which are easily transformed into dicarbonyls Cu+(CO)2 (2178 and 2150 cm 1)[ 1,2],
The coadsorption of CO and ammonia (with the different saturation of the Cu+ cations with NH3 molecules) has been followed. The ammonia molecules number interacting with one Cu+ site determined in the quantitative IR experiments was following NH^Cu^ 0.5, 1, 1.8. The interaction of CO with copper sites in zeolites CuZSM-5 containing NH^Cu^ 1.8 and NH^Cu^ I (Fig.l, spectrum b and c) results in the appearance of the monocarbonyl bands and Cu+(CO)(NH3) and Cu+(CO)(NH3), 8 at 2133 and 2100 cm'1, respectively. The CO frequency in Cu+(CO)(NH3)n adducts is distinctly lower than in monocarbonyls without ammonia molecules Cu+(CO) (2157 cm1). Such important CO bond activation is suggested to be realized by the electron transfer from electron donor ammonia molecules via Cu+ to antibonding it orbital of CO.
The coadsorption of CO and pyridine (Fig.l, spectrum d) also consequences in the development of the band of the Cu+(CO)Py adducts (at 2085 cm1). The red shift (Av = 72 cm'1) from the position of the monocarbonyls Cu+(CO) (2157 cm'1) is more pronounced in comparison to the rich ammonia Cu+(CO)(NH3)i 8 adducts. It means that one pyridine molecule is more effective electron donor than two ammonia molecules. The short evacuation at room temperature results in the disappearance either the Cu+(CO)Py (the 2085 cm'1 band) or Cu+(CO)(NH3), 8 (the 2100 cm'1 band) - spectra not shown - whereas the Cu+(CO) band (at 2157 cm'1) does not restore. Therefore the molecules of CO are supposed to be weakly bonded into both of Cu+(CO)Py and Cu+(CO)(NH3)| 8 adducts, they are easily removed.
The results of coadsorption of CO and H2O (Fig. 2, spectra a - e) have been found as the most interesting. Similarly as for ammonia and pyridine, the red shifted band of the carbonyl Cu+(CO)(H2O)n adducts was detected. The position of this band depends on the number of water molecules bonded into Cu+(CO)(H2O)„ adducts. The highest activation of CO bond was observed for maximum amount of water in CuZSM-5 (i.g. Cu+ cations) - the CO band at 2110 cm'1. The lower number of H2O molecules is, the activation of CO bond is less pronounced and the red shift of the band of Cu+(CO)(H2O)„ adducts is smaller. What is interesting, the evacuation at room temperature consequences in the disappearance of the red shifted component Cu+(CO)(H2O)n while the monocarbonyl band Cu+(CO) at 2157 cm'1 is restored (Fig. 2, spectra f - i). Contrary to the Cu+(CO)Py and Cu+(CO)(NH3)| 8 adducts where the CO molecules where weakly bonded to Cu+ cation, in Cu+(CO)(H2O)n complexes the water molecules are weekly bonded to Cu+(CO).
147

NOEA 2011
Zakopane 4-7 September 2011
Figurel. The IR spectra of CO sorbed in CuZSM-5: (a) without preadsorbed molecules, (b) containing NH/Cu* = 1, (c) containing NHj/Cu* = 1.8, and (d) with pyridine coadsorbed.
Figure2. The IR spectra recorded upon the sorption of CO in CuZSM-5 without H2O preadsorbed (a), with H2O preadsorbed (b - e), and after the evacuation at room temperature (f- i).
This study was sponsored by the Ministry of Science and Higher Education, Warsaw, Poland (project No. N N204 017039).
[ 1 ] G. Hiibner, G. Rauhut, H. Stoll, E. Roduner, Phys. Chem. Chem. Phys. 4 (2002) 1073
G.T. Palomino, S. Bordiga, A. Zecchina, G.L. Marra, C. Lamberti, J. Phys. Chem. B 104 (2000) 8641
148

NOEA20I1
Zakopane 4-7 September 2011
PS16
##### The simultaneous SCR of N2O and NOX on Co-Na-MOR using CH4 alone as the reducing agent
##### M. C. CAMPA1, V. INDOVINA1’2, D. PIETROGIACOMI1,2
1 Istituto per lo Studio dei Materiali Nanostrutturati-CNR, do Dipartimento di Chimica,
"Sapienza" Universita di Roma, Piazzale Aldo Moro 5, 00185 Roma, Italy.
2 Dipartimento di Chimica, “Sapienza ” Universita di Roma,
Piazzale Aldo Moro 5, 00185 Roma, Italy
Uhde’s proprietary EnviNOx® process performs the tail-gas abatement of N2O and NOK over iron containing zeolite catalysis. In cooperation with Siid-Chemie, Uhde has developed special iron-exchanged zeolite catalysts for use in the EnviNOx® process [I]. Iron-containing MFI zeolites are active for N2O abatement with various hydrocarbons (CH4, C2H6, C2H4, C2H2> C3H8, C3H4) [2] and with CH4, CO, or CH4+CO mixtures [3], These catalysts and analogous iron-containing catalysts are poorly active for N2O decomposition [3,4] and inactive for NOX abatement with CH4 in the presence of excess O2 [5]. A drawback with the iron-containing zeolites is the CO formation during N2O or NOX abatement using hydrocarbon reducing agents [2,6-8].
Co-Na-MOR catalysts are (i) active for N2O decomposition [4,9,10], (ii) active and selective for NOX abatement with CH4 in the presence of excess O2 [ 11 ], and (iii) active and selective for N2O abatement with CH4 in the presence of excess O2 [12]. At variance with iron-containing zeolites, on Co-Na-MOR in the selective catalytic reduction of NO or N2O with CH4 no CO formed [11,12]. Because Co-Na-MOR catalysts are active for both the SCR of NOX and the SCR of N2O with CH4, in this paper we investigated the activity of these catalysts for the simultaneous SCR of N2O and NOX using CHi alone as the only reducing agent.
The catalyst we tested, Co-Na-MOR-9.2-104, was a portion of that we have previously characterized by FTIR, using CO or NO as probe molecules, and volumetric adsorption of CO [11-13]. In preliminary experiments, we checked that the activity of this catalyst for (i) N2O decomposition, (ii) CH4+N2O, (iii) CH4+O2, (iv) SCR of NO with CH4 and (v) SCR of N2O with CH4 matched that of the same sample investigated previously for the same reactions [11,12],
The catalyst was prepared by ion-exchange of Na-MOR at 350 K by contacting a weighted amount of MOR with an aqueous solution of acetate of cobalt. To obtain this extensively exchanged sample, three exchange procedures were run in sequence. Sample is labeled as Co-Na-MOR-9.2-104, where 9.2 is the Si/Al ratio value, and 104 is the analytical metal ion exchange percentage, calculated assuming that one Me corresponded to two Al atoms. The catalytic activity for the various reactions was studied in a flow apparatus with GC analysis of reactants and products.
The results show that Co-Na-MOR is active for the simultaneous SCR of N2O and NOX using CH4 alone as the reducing agent (Fig. 1).
149

NOEA 2011
Zakopane 4-7 September 2011
Figure I. Percent NO conversion, percent N2O conversion and percent CH4 conversion, as a function of temperature on Cu-Na-MOR-9.2-I04.Composition mixture/ppm : NO/N2O/CH4/O2 - 4000/4000/4000/20000
111 Brochures of EnviNOx, are available at http://www.uhde.biz
1. M.A.G. Hevia and J. Perez-Ramirez. Environ. Sci. Technol. 42 (2008) 8896-89(X)
2. M.N. Debbagh, C. Salinas Martinez de Lecea, J. Perez-Ramirez, Appl. Catal. B 70 (2007) 335-341
3. Y. Li, J.N. Armor, Appl. Catal. B I (1992) L2I-L29
4. V.l. Parvulescu, P.Grange, B. Delmon, Catal. Today 46 (1998) 233-316
5. X. Feng, and W. K.Hall, J. Catal. 166 (1997) 368-376
6. H.-Y. Chen, W.M.H. Sachtler, Catal. Today 42 (1998) 73-83
7. H.-Y. Chen, X. Wang, W.M.H. Sachtler, Appl. Catal. A 194-195 (2000) 159-168
|9] F. Kapteijn, J. Rodriguez-Mirasol, J.A. Moulijn, Appl. Catal. B 9 (1996) 25-64
[10] M.C. Campa, V. Indovina, D. Pietrogiacomi, Appl. Catal. B 91 (2009) 347-354
[ 11] M.C. Campa, I. Luisetto, D. Pietrogiacomi, V. Indovina, Appl. Catal. B 46 (2003) 511-522
1. M.C. Campa. V. Indovina, D. Pietrogiacomi, Appl. Catal. B, submitted
2. V. Indovina, M.C. Campa, D. Pietrogiacomi, J. Phys. Chem. C 112 (2008) 5093-5101
150

NOEA2011
Zakopane 4-7 September 2011
PS 17
##### In situ FT-IR spectroscopic investigation of gold supported on tungstated zirconia as DeNOx catalyst
##### M, KANTCHEVA1, M. MILANOVA1
Department of Chemistry, Bilkent University, 06800 Ankara, Turkey,
e-mail: margi@fen.bilkent.edu.tr (M. Kantcheva)
Recent investigations have shown that a combination of a noble metal and W oxide generates catalytic systems active in the SCR of NOX with CO [1,2]. Herein, we report the results of spectroscopic characterization of gold catalyst supported on tungstated zirconia. The Au/WOx-ZrO2 sample was prepared by cationic adsorption using [Au(en)2]CI3 as the precursor (en=ethylenediamine). This method was developed first by Guillemot et al. [3] for the introduction of gold on oxide supports with a point of zero charge below 5. In order to evaluate the potential of a new material as a catalyst in the process of CO-SCR of NOX, it is important to investigate the interaction of the reactants with the surface. For that purpose we used in situ FT-IR spectroscopy to study the adsorption of CO and its coadsorption with oxygen and NO over Au-promoted and Au-free tungstated zirconia.
Sample preparation.
Tetragonal ZtO2 was prepared according to the procedure described in [4]. Tungstated zirconia containing 18 wt% of WO3 (denoted as 18WZ-CP) was synthesized by co-precipitation [5], Gold was deposited by cation adsorption from aqueous solution of [Au(en)2]3+ complex at pH=9.6 and room temperature [3],
Sample characterization.
XRD analysis was performed on a Rigaku Miniflex diffractometer with Ni-filtered Cu Ka radiation (%= 1.5405 A). The DR-UV-Vis spectra were recorded under ambient conditions with a fiber optic spectrometer AvaSpec-2048 (Avantes) using WS-2 as a reference. The X-ray photoelectron spectra were obtained using unmonochromatized Al Ka (1486.6 eV) radiation in a VG ESCALAB MK 11 electron spectrometer. The FT-IR spectra were recorded using a Bomem Hartman & Braun MB-102 model FT-IR spectrometer with a liquid-nitrogen cooled MCT detector at a resolution of 4 cm'1 (100 scans). The self-supporting discs (-0.01 g/cm2) were activated in the IR cell by heating for 1 h in a vacuum at 400°C, and in oxygen (100 Torr, passed through a trap cooled in liquid nitrogen) at the same temperature, followed by evacuation for 1 h at 400°C. The spectra of adsorbed gases were obtained by subtracting the spectra of the activated sample from the spectra recorded. The sample spectra were also gas-phase corrected.
According to the XRD data all of the samples have the structure of tetragonal zirconia. The average size of the gold particles is around 8 - 9 nm as calculated by using Scherrer equation and the main gold diffraction line of 20 = 38.2°. The optical spectra of the Auconlaining sample indicate that gold hinders the LMCT transition (O2->Wfrt) suggesting that the gold particles are in a contact with the WOX species. According to the XPS data, the Au/18WZ-CP sample contains in addition to Au°, W(VI) and Zr(IV), some amount of W(V) and Zr(lll). The surface concentration of gold on Au/ZrO2 and Au/18WZ-CP samples is 0.2 and 0.3 at %, respectively.
151

NOEA 2011
Zakopane 4-7 September 2011
Figure I. FT-1R spectra collected at various temperatures during the interaction between CO (10 Torr) and nitrate species adsorbed on the catalyst surfaces
Fig. I displays the FT-1R spectra obtained during the interaction of nitrate species adsorbed on the surfaces of Au/18WZ-CP and Au/ZrO2 catalysts with CO (10 Torr) at various temperatures. The surface nitrates were generated by adsorption of a (10 Torr NO +25 Torr 02) mixture at 25°C for 20 min followed by evacuation for 20 min at the same temperature. The contact of the samples containing pre-adsorbed NO< ions with CO at room temperature causes the formation of NCO species adsorbed on gold particles. In the case of the Au/18WZCP catalyst, the isocyanates disappear at 200°C simultaneously with the NO2 that is generated in the gas phase by decomposition of the surface nitrates. The NCO+NO2 reaction on the Au/ZrO2 catalyst (Fig. 1) takes place at higher temperature (250°C). In the absence of CO, gaseous NO2 over both catalysts is observed in the 25 - 250°C temperature range (the spectra are not shown). This fact supports the conclusion that NO2 is reduced by CO with the intermediacy of Au-NCO species leading to the formation of N2 and CO2. Although the higher concentration of surface nitrates on the Au/ZrO2 sample, the amounts of NCO species formed and NO2 evolved in the gas phase are lower than those observed over the Au/l8WZCP catalyst (Fig. I). This suggests that the tungstate species decrease the stability of surface nitrates making the WOx-containing catalyst more active in the NO3'+CO surface reaction. In addition the weak absorptions al 1450 and 1420 cm'1 2 3 observed in the spectrum of Au/ZrO2 detected at 250°C (Fig. 1) indicate the formation of stable polydentate carbonates which may have negative effect on the catalytic activity. No such species are found in the case of the Au/18WZ-CP sample. The NO+CO adsorption on Au/18WZ-CP catalyst in the 25 - 250°C temperature range does not cause the formation of surface nitrates and no Au-NCO species are detected under these conditions. This result implies that the nitrate species or adsorbed NO2 are essential for the generation of surface isocyanates and the oxidation of NO by oxygen is an important step. Finally, it should be noted that the Au-free 18WZ-CP sample does not catalyze the interaction between adsorbed nitrates and CO. The evolved NO2 is present in the gas phase between 25 and 350°C.
The results of in situ FT-IR spectroscopic investigation indicate that Au catalyst supported on lungstated zirconia could be promising in the selective reduction of NOX with CO under lean conditions.
This work has been performed in the framework of a D36/003/06 COST program. The financial support ofTBAG - I09T854 Project is greatly appreciated. We thank Dr. I. Avramova for the XPS analysis. 1 2 3
[1]	M. Shimokawabe. N. Umeda, Chem. 1 >ett. 33 (2004) 534-535
[2]	M. Shimokawabe, M. Niitsu, H. Inomata, N. Iwasa and M. Arai, Chem. Ixtt. 34 (2005) 1426-1427
[3]	I). Guillemot, V. Yu. Borovkov, V. B. Kazansky, M. Polisset-Thfoin, J. Fraissard, J. Chem. Soc. Faraday Trans. 93 (1997) 3587-3591
152

NOEA20I1
Zakopane 4-7 September 2011
1. A. Adamski, P. Jakubus, Z. Sojka, Mater. Sci.-Poland 26 (2008) 373-380
2. J.G. Santicsleban, J. V. Vartuli, S. Han, R. D. Bastian, C. D. Chang, J. Catal. 168 (1997) 431441

NOE A 2011
Zakopane 4-7 September 2011
PS18
##### Co-Mn-Al mixed oxide supported on T1O2 for N2O decomposition
##### K. KARASKOVA1, Ż. CHROMCAKOVA1, S. STUDENTOVA
##### L. OB ALOV A14, K. JIRATOVA3
VŚB - Technical University of Ostrava,
1. Faculty of Metallurgy and Materials Engineering
2. Centre for Environmental Technologies, 17. listopadu 15, 708 33 Ostrava, Czech Republic
3. Institute of Chemical Process Fundamentals CAS v.v.i.,
   Rozvojova 135, 165 02 Prague, Czech Republic
Catalytic decomposition of nitrous oxide is the subject of research of many groups due to its negative impact on the environment. Our previous papers deal with Co-Mn-Al mixed oxide catalyst [1]. The aim of presented work is a preparation of Co-Mn-Al mixed oxide supported on TiO2 and evaluation of TiO2 support effect on N2O catalytic decomposition efficiency.
Series of Co-Mn-Al/TiO2 catalysts with different Co-Mn-Al oxide loading (1-25 wt%) were prepared by impregnation of crushed commercial TiO2 particles (0.16 - 0.315 mm with solution of nitrate salts (Co:Mn:Al molar ratio of 4:1:1) and following drying and calcination (4 hours at 500 °C in air). Samples were assigned according to content of Co-Mn-Al oxide. For comparison, the commercial TiO2 and unsupported Co-Mn-Al mixed oxides prepared by two different methods (Co-Mn-Al-carb, Co-Mn-Al-nitr) were used. The Co-Mn-Al-nitr catalyst was prepared by calcination of corresponding nitrates, the Co-Mn-Al-carb catalyst by mechanochemical reaction of Co, Mn, Al nitrates with NH4HCO3. All prepared samples were characterized using various techniques (XRD, N2 adsorption/desorption measurements, TPR-H2 andTPD-NH3, CO2).
Catalytic measurements of N2O decomposition were performed in an integral fixed bed stainless steel reactor of 5 mm internal diameter (300 - 450 °C, atmospheric pressure, 0.1 mol% N2O balanced by helium, 0.1 g catalyst, GHSV 60 1 g'1 h1). Fraction with particle size of 0.160- 0.315 mm was used for catalytic measurements. The steady state of the N2O concentration level was measured. The quadrupole mass spectrometer RGA 200 (Stanford Research Systems, Prevac) was used for N2O analysis (mJz = 44).
XRD results of Co-Mn-AI/TiO2 catalysts confirmed presence of TiO2 (anatas) and Co-Mn-Al spinel­like oxides (not shown). The observed diffraction lines in Co-Mn-Al-carb and Co-Mn-Al-nitr catalysts were ascribed only to the spinel-like oxides. All samples exhibited a relatively low crystallinity with exception of Co-Mn-Al mixed oxide prepared from nitrates (Co-Mn-Al-nitr) which showed sharp and high diffraction peaks. The finding is in good agreement with the results describing their porous structure: Co-Mn-Al-nitr catalyst had much more smaller volume of micro- and mesopores, four times lower specific surface area and two limes higher mean mesopore radius (Table 1). Slight decrease in pore volume, specific surface area and mean pore radius were observed with increasing amount of Co-Mn-Al oxide in the supported catalysts.
The temperature dependences of N2O conversion are shown in Fig. 1. Pure TiO2 was completely inactive at given experimental conditions. The increase of N2O conversion with increasing amount of Co-Mn-Al oxide in Co-Mn-Al/TiO2 catalysts was observed except the 25% Co-Mn-Al/TiO2 sample. Conversion curve of N2O obtained with the catalyst prepared by calcination of Co-Mn-Al LDH precursor (Co:Mn:Al molar ratio of 4:1:1) in our previous work [1] is also included in Fig. 1 (sample Co-Mn-Al-HT-ex).
155

NOE A 2011
Zakopane 4-7 September 2011
Table I. Structural and catalytic properties of Co-Mn-AI/Tt()2 samples
Sample
‘'’BIT Vmeso
(m2g')	(cm3g')
r 2> V 3)
' meso	v micro
(nm)	(mm’g1)
4,	NA) reacted51
6",c"’	(IO6 mol/m2 of
(nm) catalyst)
TiO2	200	0.54	-		-	0
1 % Co-Mn-Al/TiO2	100	0.45	II.1	43	0.41	68.0
7% Co-Mn-Al/TiO2	95	0.42	11.4	40	0.40	5.3
14% Co-Mn-Al/TiO2	96	0.37	10.0	41	0.39	4.6
16% Co-Mn-Al/TiO2	91	0.32	9.5	39	0.39	15.0
25% Co-Mn-Al/TiO2	74	0.23	9.0	32	0.39	8.6
Co-Mn-Al- nitr	35	0.15	21.7	15	0.47	10.1
Co-Mn-Al- carb	134	0.78	12.4	58	0.36	8.4
Co-Mn-Al-HT-ex	93	0.48				12.2

11 Cumulative mesopore volume. BJH method;2’ Mean mesopore radius, BJH method;'1 Cumulative micropore volume, Horvath Kawazoe method;41 Mean micropore radius, Horvath Kawazoe method; 5) at 450 °C
The Co-Mn-Al-HT-ex and Co-Mn-Al-carb catalysts were the best samples and showed the same behavior of N2O conversion curve on reaction temperature. The Co-Mn-Al-nitr was the worst from the Co-Mn-Al mixed oxide samples mentioned above.
Figure I. Temperature dependence of N2O decomposition over Co-Mn-Al mixed oxide supported on TiO2. Conditions: 0.1 mol% N2O balanced in He, atmospheric pressure, GHSV = 601 g1 h1.
From the presented results, it is evident that specific catalytic activity expressed as reacted moles of N2O per 1 m2 of catalyst surface is nearly the same with the exception of 1% Co-Mn-AI/TiO2 catalyst, which was likely caused by big experimental error at low N2O conversions (Table 1). Titania in all
156

NOEA2011
Zakopane 4-7 September 2011
Co-Mn-AI/TiO2 catalysts acts only as a catalytic support and does not contribute to their catalytic activity. Different procedure used in preparation of the pure Co-Mn-Al mixed oxides had crucial influence on morphology of resulting materials and achieved N2O conversions. However, their specific activities were the same within the experimental error.
This work was supported by the Czech Science Foundation (project No. 106/09/1664) and EU project No. CZ. 1.05/2.1.00/03.0100 „ Institute of Environmental Technologies “.
[ 1 ] L. Obalova, K. Pacullova, J. Balabanova, K. Jiratova, Z. BastI, M. Valaskova, Z. Lacny, F. Kovanda, Catal. Today 119(2007)233

NOEA2011
Zakopane 4-7 September 2011
PS 19
##### Photocatalytic decomposition of N2O on Ag-TiCh
##### K. KOĆI1, S. KREJCIKOVA2, Z. LACNY1,0. SOLCOVA2, L. OBALOVA*
VŚB - Technical University of Ostrava, Faculty of Metallurgy and Materials Engineering,
17. listopadu 15, 708 33 Ostrava, Czech Republic
Institute of Chemical Process Fundamentals CAS v.v.i.,
Rozvojova 135, 165 02 Prague, Czech Republic
Until recently, nitrous oxide (N2O) had received little attention as an atmospheric pollutant. Its harmful impact on the environment is now well recognized. N2O plays a significant role in the destruction of the ozone layer. N2O is also a major greenhouse gas. Photocatalytic decomposition of N2O is one of the candidate methods for its removal. N2O can be reduced by the electrons generated by UV irradiation on semiconductor photocatalysts, evolving N2 and O2. Titanium dioxide (TiO2) is well known as photocalalyst for wastewater treatment, hazardous waste control, air purification, and water disinfection. However, TiO2 (anatase) exhibits a relatively high energy bandgap (3.2 eV) and can only be excited by high energy UV irradiation with a wavelength shorter than 387.5 nm. Efforts have been made to extend the light absorption range of TiO2 from UV to visible light and to improve the photocatalytic activity of TiO2 further by adding noble metals. For example, Ag can serve as successful dopant to TiO2 for increasing yields of several types of photocatalytic reactions [1], evaluation of Ag-TiO2 efficiency for N2O photocatalytic decomposition is the aim of presented work.
Silver-enriched TiO2 powder was prepared by the sol-gel process controlled in the reverse micellar environment and characterized by X-ray diffraction (XRD), nitrogen adsorption measurement and UV-Vis HL
The photocatalytic measurements of N2O decomposition were carried out in a homemade apparatus al ambient temperature. A batch annular reactor was fill with 600 ppm N2O/air mixture (volume 756 cm3, pressure 110 kPa) and illuminated by an 8 W Hg lamp with a peak light intensity at 254 nm (Ultra-Violet Products Inc., USA, 11SC-1) situated in the center of the quartz tube; the shell tube was made from stainless steel. The Ag-TiO2 powder (0.215 g) was distributed evenly over the adhesive tape located in the bottom of reactor. GC/TCD was used for the analysis of N2O. The N2O concentration level was measured before switching of UV lamp and during the irradiation.
The basic textural properties of prepared doped titania sample are summarised in Table 1 together with real Ag content. The sample possesses a relatively high surface area. XRD analysis confirmed the presence of the pure anatase crystallite structure. The absorption edge value was evaluated from UV-Vis measurement [ I ], shift to the visible light region was observed compared to pure anatase.
Table 1. Basic characterisation of prepared photocatalyst sample
Sample	Ag content (wt.%)	Sbet (m2/g)	I"max (nm)	Absorption edge (eV)
Ag-TiO2	0.725	80	1.41	2.88

1 Maximum pore radius
Figure 1 shows the time dependence of N2O conversion over Ag-TiO2. The gradual increase of N2O conversion was observed with increasing reaction time, N2O conversion was about 75 % after 24 hours. The kinetic data of N2O photocatalytic decomposition can be described by 1st rate law (Fig. 2): r = kcN()	.
, £ = 0.0509 h
159

NOEA 2011
Zakopane 4-7 September 2011
Figure 2. Evaluation of kinetic constant (lsl rate law) for N2O photocatalytic decomposition by integral method
The following mechanism of N2O photocatalytic decomposition is proposed: When illuminated by UV light with a sufficient photonic energy (hv) and an appropriate wavelength, photon-generated electrons (e~) and holes (h+) are created on the surface of the Ag-Ti()2 catalysts (Eq. 1-2). Furthermore, the photoexcited electrons and holes in the lattice are separated and trapped by the appropriate sites of Ag-Ti()2 to avoid recombination. At first, the electrons react with N2() adsorbed on the catalyst surface producing N2 and «O radicals (Eq. 3). These incipient •()' radicals react with holes to produce ()2 (Eq. 4).
160

The pholocatalytic properties of the nanocrystalline Ag-TiO2 catalyst were evaluated by pholocatalytic decomposition of N2O. Reaction kinetics was well described by Is1 rate law, which is in agreement with plausible reaction mechanism where N2O chemisorption (Eq. 3) is the rate determining step. The decomposition of N2O by photocatalysts was one of the most promising methods, since N2O can be decomposed to innocuous substances by irradiating it with UV light at room temperature, i.e. at the conditions when N2O thermal catalytic decomposition does not proceed.
This work was supported by the Grant Agency of the Czech Republic 203/08/H032 and EU project No. CZ. 1.05/2.1.00/03.0069 ,,ENET“.
[ 1 ] K. Koći et al, Appl. Catal. B 96 (2010) 239

NOEA201I
Zakopane 4-7 September 2011
PS20
##### Effect of V concentration in niobium-rich V-O-Nb/anatase catalysts on their activity in ammonia assisted DENOX
##### P. KORNELAK1, A. BIAŁAS*, D. RASIŃSKA1, J. CAMRA2, W. ŁASOCHA1 ,W. ZHANG3, D. SU3, A. WESEŁUCHA-BIRCZYŃSKA1,
##### M. NAJBAR1*
1 Faculty of Chemistry, Jagiellonian University, 3 Ingardena St.,
30-060 Kraków, Poland, *mnajbar@chemia.uj.edu.pl
Faculty of Materials Science and Ceramics, AGH University of Science and Technology,
30 Mickiewicza Av.., 30-059 Krakow, Poland
Department of Inorganic Chemistry Fritz-Haber-Institut der Max-Planck Geselleschaft,
Faradayweg, 4-6, D-14195 Berlin, Germany
Anatase supported vanadia-niobia catalysis are frequently proposed as alternative for anatase supported vanadia-tungsta commercial ones for NO reduction by ammonia.
The effect of niobium on the catalyst activity is not well understood by now. According to Ziolek [1] the addition of niobium to vanadia-titania catalyst improves their activity as a result of increasing amount of the surface redox and acid sites. Tanabe [2] have shown that addition of Nb to V2O5/TiO2 catalysts distinctly improves their low temperature activity and stability in NO SCR by ammonia. That conclusion has been supported by earlier Japan patents [3-6]. Those patents has also revealed an increase of mechanical strength of the catalyst due to Nb addition. Wachs et al. [7] have investigated anatase supported vanadia and niobia catalysis by Raman spectroscopy. They have claimed the absence of crystalline Nb2O5 and occurrence of two-dimensional overlayers, retarding the loss in surface area of the titania support, either on the Nb2Oj/TiO2 or V2O5/Nb2O5/TiO2 catalysts surfaces. Schneider et al. [8] have found surface reconstruction of vanadia-niobia catalysts obtained by sol-gel method during calcinations at 723K. They have revealed that reconstruction, resulting in the vanadia patches and three dimensional structures formation, caused increase of the catalyst activity in NO SCR by NH3.
It is known that vanadia forms solid solutions in niobia [9,10], Thus, it could be expected that vanadium sites in niobia overlayers also show some catalyst activity in NO SCR by ammonia. To follow up this expectation, two titania supported vanadia-niobia catalysts with high niobia predominance (4.5 wt. % Nb2O5) and different vanadia content (1.1 or 2.2 wt.% V2O5) were obtained. The surface physico-chemical properties and SCR activity of these catalysts were investigated to explain the dependence of the catalyst activity on a number and a degree of oxidation of vanadium atoms in the surface Nb-O-V species.
The anatase-supported V-O-Nb catalyst with atomic V:Nb ratio equal to 1:2.8 (1.1 wt.% V2O5 - 4.5 wt. % Nb2O5/TiO2) was obtained by sol-gel method from titanium isopropoxide, vanadyl isopropoxide and niobium ethoxide. This catalyst was used for obtainment of another one with twice higher content of vanadium by the deposition of the oxy-hydroxy vanadium sols on its sol particles.
The characterisation of both the catalysts was performed using XRD, HRTEM, XPS and Raman spectroscopy. The results obtained for catalyst with 1.1 wt% V2O5 show the presence of the epitaxial layers of Nbl8V4O55 mixed oxide phase on anatase nanocrystallites surface. However, the results for catalyst with 2.2wt% V2O5 reveals the transformation of epitaxial layers of Nbl8V4O55 into V2Nb6O|9 nanocrystallites during the second step of its synthesis. The deconvolution of the V 2p3/2 peaks in XP spectra allowed to find that vanadium in the surface nannolayers of both the catalyst is present mostly at low oxidation states (I and III).
The results of the catalytic test show that niobia-rich catalysts are active in NO SCR by ammonia mainly due to NO decomposition on interstitial vanadium cations with low oxidation state. NO decomposition is the rate determining step of NO SCR by ammonia at relatively low temperature and the
163

NOEA20II
Zakopane 4-7 September 2011
active oxygen is not involved in oxidation-induced surface V segregation. The surface vanadium segregation results in vanadia species formation. The segregation appeared in catalyst with I. I wt% V2O5 content above 300°C and in the second catalyst, with twice vanadia loading, above 350°C. Ammonia is oxidised on vanadia-like species by molecular oxygen.
The comparison of the phase and chemical compositions of the catalysts with their NO SCR activity allows to think that the surface interstitial vanadium atoms with low oxidation states in the mixed V-O-Nb phases play the role of the active sites. The oxidation-induced surface segregation of the interstitial vanadium atoms, resulting in vanadia species formation, is postulated to be responsible for the ammonia oxidation.
1. M. Ziółek, Catal. Today 78 (2003) 47
2. K. Tanabe, Catal. Today 8 (1990) 1
3. H. Ulsunomiya, K. Soga, K. Shimazaki, Y. Milo and M. Aoki, S. Haseba, H. Miki and M. Masaki, Ger. Offen, 2634279 (1976)
4. H. Ulsunomiya, K. Shimazaki, K. Soga, Y. Milo andM. Aoki, Japan Patent Kokai, 52-151688 (1977)
5. E Kurosawa, Japan Patent Kokai, 54-52692 (1979)
6. S. Haseba, S. Ito, Y. Mito and T. Hirano, Japan Patent Kokai, 55-28718(1980)
7. E. Wachs, J.-M. Jehng and F. D. Hardcastle, Solid State Ionics. 32/33 (1989) 904
8. M. Schneider, U. Scharf, A. Wokaun and A. Baiker, J. Catal. 150 (1994) 284
9. R. H. H. Smith, K. Seshan, H. Leemreize, J. R. H. Ross, Catal. Today 16 (1993) 513
10. Z. Zhao, X. Gao, I. E. Wachs, J. Phys. Chem. B 107 (2003) 6333
164

NOEA2011
Zakopane 4-7 September 2011
PS21
##### Alloying effect on NO direct decomposition over high surface area Rh/AhOa catalysts
##### A. PIETRASZEK1, P. Da COSTA2, P. KORNELAK1, B. AZAMBRE3,
##### L. ZENBOURY3, M. NAJBAR1
1 Department of Chemistry, Jagiellonian University, 3 Ingardena St., 30-060 Kraków, Poland
2 Laboratoire de Reactivite de Surface, Universite P. et M. Curie,
Place Jussieu, 75252 Paris Cedex 05, France
Laboratoire de Chimie et Applications, Universite Paul Verlaine de Metz - IUT
Chimie.rue Victor Demange 57500 Saint Avoid
A removal of NO, (NO and NO2) from oxygen-containing off-gases of stationary sources of emission such as power and heat plants, nitric acid factories, waste-incineratorsand stationary Diesel engines is the fundamental problem of environmental catalysis.
Nitrogen oxides NO, in those off-gases contain above 90% of NO. Nitric oxideis formed from air by endothermic N2 oxidation at temperatures above 1000°C. Thus, NOis thermodynamically unstable molecule, with the high, positive formation enthalpy, it could decompose to N2 and O2 at low temperatures (between 20 and 700“C).
The direct NO decomposition seems to be the best way of NO removal from off gases because of practical, environmental as well as economical reasons. This process does not require reducer that allows to avoid secondary pollutants like mildly oxygenated hydrocarbons, CO, NH3 or even cyanate and isocyanate. However, in the case of direct NO decomposition N2Ocan be formed besides N2 because of two possible paths of the process:
2NO -> N2 + O2
2NO —> N2O +‘/2 O2.
Oxide supported precious metal catalysts are known to be the most active in direct NO decomposition among the metal catalysts supported on metal oxides.
The aim of this research was to investigate the NO decomposition in the oxygen presence over Rh/5-AI2O3 catalysts with different loadings (0.06, 0.12 and 0.18wt.%). The trial was undertaken to determine the active sites of this process.
High surface area alumina was obtained with the sol-gel method. The solution of RhCl3*3H2O in water was next added to the alumina sol solution. The precursor of the 0.06wt.%Rh/Al203 catalyst was obtained by solution evaporation, calcination and reduction in a hydrogen. The 0.12wt.%Rh/AI2O3 catalyst was synthesised from 0.06wt.%Rh/AI203 oneby repeating the same procedure. The 0.18wt.%Rh/8Al2O3 catalyst was obtained in the same way from 0.12wt.%Rh/Al2O3 one.
The catalysts were characterised by measurements of BET specific surface area TPD of CO and NO adsorbed as well as DRIFTS of the CO adsorbed. The BET specific surface areas was found to increase continuously with deposition of two first portion of 0.06wt.% Rh on the alumina support and to decrease with the addition of the third such portion. Unexpected increase of the specific surface area with addition of third portion suggests the distinct separation of the Al-Rh alloy nanocrystallites from the larger alumina ones. The DIRFT spectraof the adsorbed CO clearly show the presence of Al-Rh alloy with atomically dispersed rhodium and rhodium modified alumina of enhanced oxygen mobility on the catalyst surface.
The NO direct decomposition in reaction mixture containing 200ppm NO, 1600ppm methane, 7% oxygen and helium was investigated under steady-state conditions in 200 - 400°C temperature range at GHSV=20000h '. The steady-state experiments were performed in a quartz flow reactor using 0.2g of the catalyst in the direction from 400 to 200°C, after pre-treating the catalysts in the reaction mixture at 500°C .The NO conversion and the selectivity to N2 as a function of temperature are presented in Fig. 1.
165

NOEA 2011
Zakopane 4-7 September 2011
Fig. I. The NO conversion (a) and selectivity to N2 (b) on the 0.06 Rh/ SALOj , 0.12 Rh/ <)A12Oj and 0.18 Rh/ dAl2Ot catalysts a function of temperature (0.200g; 2(X)ppm NO, 1600ppm CH4 and 7 %O2; GHSV=20000h')
The highest NO conversion and the highest selectivity towards N2 observed on ().18wt.%Rh/8Al2O3 catalyst at temperature range 200 - 300"C can be ascribed to the direct NO decomposition over separated Al-Rh alloy nanocrystallites. The surface Rh atoms with enhanced electron density on the surface of the Al-Rh alloy nanocrystallites are discussed to be active sites in direct NO decomposition. The drop of the activity and selectivity above 300°C distinctly shows a deep surface reconstruction.
To check stability of the surface structure of the ().18wt.%Rh/8AI2O3 catalyst during the effective direct decomposition process at 200°C, the long-term (60 h) experiment was performed on the catalyst pre-treated at 400°C in the mixture of 15()ppm NO and 7%()>/He. The NO conversion to nitrogen was found to stay at the same level during 60 h and to be closed to that achieved at 200°C in the steady-state experiment presented in the Fig. 1.
166

NOEA2011
Zakopane 4-7 September 2011
PS22
##### NO decomposition over Mo-V oxide bronzes
##### P. KORNELAK1, M. ŁABANOWSKA1, W. MACYK1, M. TOBA2, I. NAZARCZUK1, M. NAJBAR1
1 Department of Chemistry, Jagiellonian University, 3 Ingardena St., 30-060 Kraków, Poland
1 National Institute of Materials and Chemical Research,
1-1 Higashi, Tsukuba, Ibaraki 305, Japan
A precursor of an anatase-supported V-O-Mo catalyst with V:Mo:Ti = 1:9:90 was prepared by sol-gel method from water solutions of (NH4)6Mo7024-4H20 and VO(NO3)2 as well as 6% TiO2 sol solution. A precursor of an anatase-supported V-0 catalyst with V:Ti =1:9 was prepared by sol-gel method from water solutions of VO(NO3) and 6% TiO2 sol solution. A precursor of an anatase-supported Mo-0 catalyst with Mo:Ti =1:9 was prepared by sol-gel method from water solutions of (NH4)6Mo7O24'4H2O and 6% TiO2 sol solution.
To obtain the catalysts the precursors were calcinated at 773 K in air for 3 hours. The catalysts were characterized by measurement of a nitrogen adsorption, EPR spectra, , and DR UV-Vis spectra and DRFTIR spectra of NO adsorbed. The activity of the catalysts was measured in u-tube quartz flow reactor on line with GC/MS equipped with DB-1 capillary column.
Figure 1. DRFTIR spectra ofV-O-Mo/TiO2 (a), MoOx/TiO2 (b) and V2O/TiO2 (c) catalysts activated in He at 723K and next subjected to interaction with NO at room temperature (200ppm NO/He, 60cm3/min)
The specific BET surface areas of all the catalysts are similar and close to 110 m2/g.
An EPR spectrum of V2Os/TiO2 catalyst registered at 77 K consists of three signals: two of them exhibit hyperfine structure characteristic for V(IV) species the third signal is a broad, structureless line.
167

NOEA 2011
Zakopane 4-7 September 2011
The parameters of the first signal are similar to those of crystalline vanadia. Two other signals are ascribed to V (IV) substituted forTi in anatase structure.
An EPR spectrum of the MoO3/TiO2 catalyst registered 77 K reveals three signals from Mo(V) species and one from Ti (III). The first signal is ascribed to Mo(V) in surroundings of oxygen atoms more symmetrical than that in orthorhombic MoO3. The next two signals arc similar to those reported for interstitial Mo(V) in TiO2 . Ti(III)species are formed as a result of Mo(V) substitution for Ti(lV) in anatase structure.
In a spectrum of the mixed V-O-Mo catalyst six superhyperfine lines with A = 1.6 are overlapped on the hyperfine lines of vanadia indicating the interaction of an unpaired electron localized on vanadium with nuclear magnetic moment I =5/2, of 95,97Mo nuclei. This fact confirms incorporation of molybdenum in vanadia. A new signal from V (IV) appears in room temperature spectrum. This signal increases slightly with a catalyst reduction and drastically with its reoxidation. Ils behavior strongly suggests that it comes from V-Mo oxide bronze containing interstitial vanadium ions in molybdena-like structure. Surface interstitial vanadium atoms occurs as a vanadyl species containing V(V) and exposing oxygen at the surface while bare vanadium ions at lower oxidation states arc present in subsurface layers and in the bulk of bronze nanocrystallites. The reduction may cause some additional filling of the surface interstitial positions with surface vanadyl species at the cost of the surface vanadia species. However, reoxidation is expected to cause the replacement of the interstitial V cations with oxidation degree lower than IV from the bulk to surface of bronze nano- crystallites were they adsorb oxygen forming vanadyl species.
Results of DR UV-Vis measurements confirm presence of Ti(III) and Mo(V) species in the fresh, reduced and oxidized V-O-Mo catalyst. A lack of absorption characteristic for crystalline V2O5 reveals predominant formation of V-Mo oxide bronze containing vanadium at oxidation degrees lower than IV.
The DRFTIR spectra of NO adsorbed on the surface of the activated catalysts are presented in Fig. 1.
Peaks at 1813 and 1713 cm'1 observed only in DRFTIR spectrum of the mixed V-O-Mo catalyst are commonly ascribed to symmetric and asymmetric vibration in dinilrosyl species.
The results of the catalytic tests show that direct NO decomposition proceeds mostly as a results of the interaction between NO groups in dinilrosyl species formed on the surface of the V-O-Mo catalyst.
Publication co-financed by the European Regional Development Fund under the Innovate Economy Operational Programme 2007-2013, POIG.01.01.02-12-112/09 project.
168

NOEA 2011
Zakopane 4-7 September 2011
PS23
##### Effect of surface potassium doping and NOX addition on catalytic activity of iron and cobalt spinels in soot combustion
##### P. LEGUTKO1, P. STELMACHOWSKI1, A. KOTARBA1, Z. SOJKA1
1 Faculty of Chemistry, Jagiellonian University, 3 Ingardena St., 30-060 Krakow, Poland
Environmental pollution is an actual problem of today’s metropolises. In this aspect particulate matter emitted from diesel engines is paid particular attention because of its carcinogenicity and mutagenicity. The best way of soot elimination from exhaust gases is application of DPF (Diesel Particulate Filler) technology. However, gradual accumulation of soot and resulting reduction of filter cross-section leads to decrease of the exhaust gases flow rate or even complete filter clogging. Therefore, to recover the DPF functionality, the filter has to be periodicaly regenerated. The most eficient way of soot elimination by combistion is the use of oxidation catalyst [1],[2],
It has been reported that nitric oxide (NO), which is always present in diesel exhaust, can severely influence the soot combustion process. Such effect was found for several oxide catalytic materials e.g. Ba-CuOx-CeO2 [3], La2O3, [4] and MnOx-CeO2 [5], as well as for spinel type oxides, such as ZnAl2O4 [6], BaAI2O4 [7], Cuo95Koo5Fe204 [8].
The effect of alkali promotion to soot combustion oxide catalysts has been well established [9], In particular, the influence of alkali addition (Li, Na and K) to ZrO2 [10] CaO-MgO [11] was tested in a detailed way. Nonetheless, despite the progress made the beneficial role of alkali is still not understood, mainly due to the lack of systematic studies on the well defined systems.
In the present work, the effect of potassium addition on iron and cobalt spinels in different gas feed composition: oxygen (5% O2/He), oxygen-NO (3.3% O2 and 1.7% NO/He) and in nitrous oxide (5% N2O/He) was investigated. Temperature Programmed Oxidation measurements of soot were conducted in a fixed bed microreactor consisting of a quartz tube with a sinter. Printex80 (Degussa) was used as the model soot. The soot-catalyst mixture (mass ratio 1:8) was prepared by grinding in agate mortar (tight contact). Gas flow was 60 ml/min and temperature range from RT to 900 °C (heating rate 10°C/min). The gas composition was monitored by QMS (RGA 200, SRS).
All investigated spinels are active catalysts in the oxidation of soot, however they exhibit diverse behavior in the different conditions. In the presence of 5%O2 alone the cobalt spinel CO3O4 shows belter activity than Fe3O4 and unpromoted reference catalyst (Fig. I). The effect of potassium addition was rather weak and leads to increase in soot ignition temperature in each case. Addition of NO to the feed changes the trend by decreasing the ignition temperature for iron spinels, whereas for cobalt spinel the temperature increased. Interestingly, in the presence of NO, potassium doping lead to spectacular increase of activity of all investigated catalysts. In the presence of N2O all catalysts showed substantially lower activity than in the presence of oxygen, despite that N2O is readily decomposed into N2 and surface oxygen species. Most probably it is caused by enhanced recombination of reactive adspecies, which hinders their involvement in soot oxidation.
169

NOEA2011
Zakopane 4-7 September 2011
Figure 1. Temperature of ignition of soot in different gas phase composition (O2 and O2+NO)for undoped and K-doped Fe3O4, Co3O4, (*) catalyst composition is subject to a patent application.
The obtained results confirm that NO presence has beneficial effect on soot particles oxidation. This effect may be dramatically enhanced upon promoting with potassium, reaching, at suitable oxide surface, the soot ignition temperature, as low as 160°C.
1. B. A. A. L. van Setten, M. Makkee, J. A. Moulijn, Catalysis Reviews 43 (4) (2001), p. 489
2. D. Fino, Science and Technology of Advanced Materials 8 (2007), p. 93
3. F. Lin, X. Wu, D. Weng, Catalysis Today, Article in press (doi:10.1016/j.cattod.2011.03.002)
4. M. A. Peralta, M. A. Ulla, C. A. Querini, Applied Catalysis B: Environmental 101 (2010), p. 38
5. X. Wu, F. Lin, H. Xu, D. Weng, Applied Catalysis B: Environmental 96 (2010), p. 101
6. M. Zawadzki, W. Staszak, F. E. Lopez-Suarez, M. J. Ilian-Gomez, A. Bueno-Lopez, Applied Catalysis A: General 371 (2009), p. 92
7. H. Lin, Y. Li, W. Shangguan, Z. Huang, Combustion and Flame 156 (2009), p. 2063
8. H. Lin, Z. Huang, W. Shangguan, Chemical Engineering & Technology 31 (2008), p. 1433
9. A. Aissat, S. Siffert, D. Courcot, R. Cousin, A. Aboukais, Comptes Rendus Chimie 13 (2010), p. 515
10. D. Hleis, M. Labaki, H. Laversin, D. Courcot, A. Aboukais, Colloids and Surfaces A: Physicochemical and Engineering Aspects 330, p. 193
11. R. Jimenez, X. Garcia, T. Lopez, A. L. Gordon, Fuel Processing Technology 89 (2008), p. 1160
170

NOEA2011
Zakopane 4-7 September 2011
PS24
#### TEM studies of transition metal oxide catalysts for NO decomposition
#### L. LITYŃSKA-DOBRZYŃSKA1, K. STAN1 M. KOZICKI2, M. NAJBAR2
1 Institute of Metallurgy and Materials Science Polish Academy of Sciences,
30-059 Cracow, 25 Reymonta St., Poland
2 Faculty of Chemistry, Jagiellonian University, 3 Ingardena St., 30-060 Kraków, Poland
Some oxide phases formed on the surface of the tubes and foil sheets from acid-resistant steel(lH18N9T/1.4541) during thermo-programed oxidation where found to be active in direct decomposition of nitrogen oxides contained in off-gasses from stationary sources of emission [1].
The microstructure of these oxide phases, formed in different conditions, was examined by use analytical and high-resolution transmission electron microscopy (TEM) FEI Tecnai G2 microscope at 200 kV equipped with EDAX energy dispersive X-ray (EDX) and high angle annular dark field detector (HAADF). In order to prepare TEM samples, the catalytic material was scraped from oxidised tubes or foils from acid-resistant steel and then the thin slices of it were placed on a carbon support copper grid.
The separate thin crystals, transparent for electron beam were analyzed. The a-FejO3 oxide and (NiCrFe)O4 spinel were identified based on the electron diffractions and EDX microanalysis.
In figure 1 the example of the TEM bright field image and electron diffraction pattern of a-Fe2O3 crystal is presented.
Figure 1. TEM bright field image of the a-Fe2O3 crystal and corresponding diffraction pattern (zone axis [ 110]); EDX spectrum and quantitative analysis result of the marked point
171

NOEA2011
Zakopane 4-7 September 2011
The oxide contains mainly Fe (about 40 at.%) and oxygen (about 58 at.%), although the small amount of Cr is also detected (Cu visible in the spectrum comes from the supporting grid). Because of very similar ionic radius of Fe3+ and Cr3* replacement of F3+ ions in tetrahedral positions by Cr3* ones in a-FejO3 structure is well understood.
Beside the iron oxide crystals, (NiCrFe)O4 spinel ones were found in investigated samples (Fig. 2). Results of EDX microanalysis showed that spinel contains Fe (about 33at.%), Ni (15 at.%), O (45 at.%) and small amount of Cr and Mn. It reveals the presence of the ferrite with some Cr cations substituted for Fe3+ ones in tetrahedral position and Ni2+ and Mn2+ and possibly some amount of F3+ in octahedral ones.
Figure 2. TEM bright field image of the (NiCrFe)O4 crystal and corresponding diffraction pattern (zone axis [112]); EDX spectrum and quantitative analysis result obtained for the marked point
Publication co-financed by the European Regional Development Fund under the Innovate Economy Operational Programme 2007-2013, POIG.Ol.01.02-12-112/09 project.
M. Najbar, J. Dutkiewicz, L. Lityńska-Dobrzyńska, A. Wesełucha-Birczyńska, I. Nazarczuk, S. Janiga, M. Kozicki, P. Komelak, A. Bielańska, W. Lasocha, „Simultaneous NO reduction and soot oxidation on transition metal oxide catalysts” in this Book of Abstract
172

NOEA2011
Zakopane 4-7 September 2011
PS25
##### DRIFT study of deNOx reaction over Cu/CeZrC>2 catalyst
##### A. ŁAMACZ1, A. KRZTOŃ1, G. DJEGA-MARIADASSOU1
1 Polish Academy of Sciences, Centre of Polymer and Carbon Materials, Zabrze, Poland
According to the three function model on supported metal cation [1] deNO, reaction proceeds in three assisted catalytic cycles, which are not kinetically coupled, i.e. they do not have a common adsorbed species. The model concerns a reaction feed that composition is: NO + Oxygen in excess + Hydrocarbon (HC) as reductant, where HC depends on the application. The model makes an assumption of three following functions:
Fl: NO+ 1602 = NO
F2: HC + NO2 = “oxygenates” + NO F3: 2NO + “oxygenates” = N2 + CO2 + H2O
The present work reports in situ DRIFT analyses during temperature programmed desorption of NO and deNOx reaction carried out on Cu/CeZrO2 Its purpose is to identify the surface species formed during deNOx reaction on Cu(4)/CeZrO2 and hereby confirm the particular functions (Fl, F2, F3) of the catalyst.
The diffuse reflectance FT-IR measurements were carried out in situ in a temperature cell fitted with ZnSe windows.
Temperature programmed desorption of nitric oxide (NO-TPD) was preceded by 40 minute adsorption of 250 ppm of NO on Cu(4)/CeZrO2 at room temperature. The adsorption was carried out in the absence and in the presence of oxygen (250 ppm NO + 5 vol% O2). NO-TPD experiments were carried out in flowing Ar. Spectra of catalyst surface during NO-TPD were collected at 50, 100, 200, 300 and 350°C, after 20 minutes of each isotherm. The reference spectra - of fresh Cu(4)/CeZrO2 - were acquired in flowing Ar at 50,100,200, 300 and 350°C. Before all tests, the catalyst was heated ex situ at 550°C for 2 hours in order to eliminate from its surface nitrates and carbonates.
Toluene adsorption on Cu(4)/CZ surface was studied by diffuse reflectance FT-IR during 80 minutes of catalyst exposure to 250 ppm of C7H8 in Ar, at 250°C. Spectra of catalyst surface during 80 minutes of exposure to 250 ppm NO + 250 ppm C7H8 + 5 vol % O2/ Ar (deNOx reaction) were also collected at 250°C. The absorbance spectra were obtained by dividing single beam spectra of the catalysts in the proper gas mixture by the spectrum of fresh catalysts, collected at 250°C in flowing Ar.
Figure 1 shows in situ DRIFS of Cu(4)/CeZrO2 during toluene adsorption (black) and deNOx reaction (red), both carried out at 250°C. Il is observed, that the characteristic bands of toluene (3110-2700 cm'1) adsorbed parallel to the catalyst surface (no out of plane C-H in 900-650 cm’1 region) decrease significantly when the catalyst is exposed to the mixture of NO+C7H8+O2/Ar. It implies that C7H8 is consumed in deNOx reaction.
Moreover, the adsorption of toluene results in its oxidation by ceria-zirconia and CuO to CO2, which adsorbs on the catalyst surface giving carbonates. According to Jacobs [2], the bands at 1504, 1360, 1066, 1014 cm’1 can be assigned to different types of surface carbonates. The same author ascribes adsorptions at 2933, 2845, 2723, 1559, 1553, 1542, 1371, 1362 and 1248 cm’1 to surface formates. Carbonates are undesirable surface species during deNOx reaction, because they may block the active sites of the catalyst. As observed on deNOx spectrum (red) the intensity of bands ascribed to surface carbonates and formats is much lower than on spectrum during toluene adsorption (black). Therefore, it is shown in Figure 1 that active sites for deNOx reaction on Cu(4)/CeZrO2 do not suffer inhibition by carboxylate species. During adsorption on Cu(4)/CcZrO2, toluene can also undergo mild oxidation to oxygenates (alcohols, aldehydes, ketones, carboxylic acids) that can yield dimerization. DRIFT spectrum collected during hydrocarbon adsorption shows the formations of benzaldehyde (2740 and 1653 cm’1), phthalic anhydride (1829, 1793, 1159 and 1132 cm'1) and benzoquinone (1653 cm’1) [3] on catalyst surface. Toluene is activated on the catalyst surface to benzyl species, which react with the surface of Cu(4)/CeZrO2 giving benzaldehyde, and
173

NOEA2011
Zakopane 4-7 September 2011
this can be successively oxidized to carboxylate species (e.g. formates). The oxygenates on catalyst surface are not observed in the presence of NO and O2, what indicates that they are consumed by NO in the function 3 (F3) of deNOx process. This function takes place on copper cation. In the case deNOx reaction, the additional bands are observed: in the region 1600-1520 cm'1 2 3 4 - corresponding to NO3 species and at 1736 and 1694 cm’1 - attributed to NO adsorbed on copper cation [4],
Figure 1. Toluene adsorption (black) and deNOx reaction (red) (NO+Crfig+OfAr) on Cu(4)/CeZrO2
In situ DRIFTS of deNOx reaction, as well as associated to it NO-TPD and toluene adsorption allow to investigate the mechanism of NO reduction by selected hydrocarbon and highlight the chemical modifications of catalyst surface. Presented above DRIFTS spectra obtained during catalyst exposure to the mixture of NO+O2+C7Hj proved the presence of surface nitrate species on Cu(4)/CeZrO2, being the product of surface NO oxidation (first function of deNOx). Oxygenates that are produced in the second function of deNOx are utilized in the third function by NO, therefore their presence was not observed on Cu(4)/CeZrO2 surface. 1 2 3 4
[1]	G. Djćga-Mariadassou, Catal. Today, 90 (2004) 27
[2]	G. Jacobs, R.A. Keogh, B.H. Davis J. Cat 245 (2007) 326-337
[3]	G. Busca, Catal. Today. 27 (1996) 457-496
[4]	Z. Wu, Z. Sheng, Y. Liu, H. Wang, J. Mo J. Haz. Mat. 185(2011) 1053-1058
174

NOEA2011
Zakopane 4-7 September 2011
PS26
##### XRD study of oxide Ni-Fe-Cr catalysts for NO decomposition
##### W. ŁASOCHA1, A. RAFALSKA-ŁASOCHA1,1. NAZARCZUK1, M. NAJBAR1
1 Faculty of Chemistry, Jagiellonian University, 3 Ingardena St., 30-060 Kraków, Poland
Oxide layers, which showed high activity and selectivity to nitrogen in the direct decomposition of NO in the presence of large amounts of oxygen were produced on the surface of the foil strips and tubes made of acid-resistant austenitic steels. These oxide layers were created using several heating programs with the use of gas mixtures with different oxygen content.
Among others methods, X-ray powder diffraction (XRPD) was used to determine the phase composition of the layers. The study was conducted either on powder samples obtained by scraping the surface oxide layer of oxidized tubes or directly on the pieces of the oxidized foils of stainless acid-resistant austenitic steels.
Such studies show some technical difficulties due to: small size of the samples, thin layers of the tested product, metallic substrate - giving strong, often very little selective, diffraction pattern.
In order to obtain optimal diffraction patterns, the following measurement setup was used: diffractometer X'Pert PRO MPD, 2-d detector PIXCEL, the Bragg-Brentano reflection geometry. Holder for transmission measurements with the sample sandwiched between layers of thin film, with very low X-ray scattering was used.
Diffraction patterns were analyzed by HighScore program, using PDF-4 + (ICDD) database. For materials for which, the RIR parameters are deposited in PDF-4+ database, the program allows a semi-automated quantitative phase analysis.
Such measuring setup will ensure good quality of the obtained results, and thus the certainty and reliability of carried out analysis. For example in the figure below we give the results of phase analysis of powder samples for the oxide phase which was scratched from the surface of the tube made of acid-resistant austenitic steel 1HI8N9T / 1.4541 subjected to 7 heating cycles consisting of thermo-programmed heating to a temperature of 840°C at a rate of 4 K/min and subsequent annealing at this temperature for 4 hours.
Marked peak positions of a-Fe2O3 phase and spinel phase containing Cr, Fe and Ni indicate the presence of these phases in the oxide layer formed on the surface of the oxidized tube made of 1H18N9T /1.4541 steel.
The presence of these phases has been confirmed by the results of electron diffraction (SAD) and Raman spectroscopy and indirectly by the results of Energy Dispersive X-ray Spectroscopy (EDS) and X-ray Photoeleclron Spectroscopy (XPS).
175

NOEA2011
Zakopane 4-7 September 2011
Figure 1. XRPD results of phase analysis of powder sample of the oxide catalyst.
Publication co-financed by the European Regional Development Fund under the Innovate Economy Operational Programme 2007-2013, POIG.Ol.01.02-12-112/09 project.
176

NOEA2011
Zakopane 4-7 September 2011
PS27
##### Modified Synthetic Spinels as Catalysts for Low Temperature deNzO
##### G. MANIAK1, F. ZASADA1, W. PISKORZ1, P. STELMACHOWSKI1,
##### A. KOTARBA1, Z. SOJKA1
Jagiellonian University, Cracow, 30-060, Poland
A large group of mixed valence metal oxides crystallizes in spinel structure with metal ions located in tetrahedral (Td) and octahedral sites (Oh). These compounds are represented by a general formula AB2O4, where, in the most cases, A and B are divalent and trivalent cations, respectively [1]. Spinels are widely investigated as potential catalysts in low temperature N2O decomposition, which runs with the cationic redox mechanism triggered by a transfer of electron density. This induces a strong correlation between the electronic properties and catalyst activity observed elsewhere [2,3], One of the most active dcN2O catalyst is based on cobalt spinel [2]which can be effectively promoted by alkali [2,4]. The aim of this work was to combine experimental methods and molecular modeling to explore the mechanistic role of the valence (+2, +3) and coordination (Td, Oh) of cobalt ions in the Co3O4 spinel. Selective structural doping with Mg, Al, Fe and surface doping with potassium were also investigated. juhl.
The spinel samples were obtained by precipitation method from the corresponding nitrate precursors. K-doping (2 atoms-nm'2) was achieved by incipient wetness impregnation from K2CO3. The samples were characterized by XRD (X’pert), SEM (Hitachi), TEM (TECHNAI, FEI), BET (Quantasorb), UV-VIS(Shimadzu), XPS (Prevac). Electronic properties were evaluated by the work function measurements using a Kelvin probe (KP 6500, McAllister). The TPSR-QMS of deN2O were performed. For all calculations, the DFT level of theory was chosen and the Vienna ab initio simulation package (VASP) [5] was used for the (100) plane.
The deN2O TPSR profiles for all samples are shown in Fig. 1. The results clearly show that complete substitution of cobalt in Td and Oh sites by Mg2+ and Al3+ ions, respectively, in Co3O4 caused decrease of catalytic activity, which is reflected in the modification in the obtained activation energies (from 63 kJ-mof1 for Co3O4, 71 kJ-mof1 for MgCo2O4, 117kJ-mor' for CoAl2O4 to 193 kJ-mof1 for MgAl2O4). Further enhancement of the catalytic activity achieved by surface doping with potassium revealed that the most pronounced effect occurs again for Co3+ ions in Oh positions (Co3O4 and MgCo2O4) confirming definitely their role as the active sites for deN2O reaction. The strong improvement of the surface reactivity observed as 50% conversion temperature lowering (AT5o% in Table I) correlates with decrease in the work function by potassium addition (A4>).
Table /. Selected structural and kinetic parameters for spinel catalysts
	CO3O4	MgCo2O4	COA12O4
Unit cell period	8.04	8.08	8.05
F^fdOO)	1.37	1.57	1.39
K adsorption / kcal- mol'1	102.1	88.9	92.1
A7 5o% 1 °C	161	133	82
A*/eV	0.49	0.09	0.05

The calculated change in surface atomic Bader charge of the K ion upon adsorption is +0.66, 0.52 and 0.58 for Co3O4, MgCo2O4 and CoAI2O4, respectively, indicating a pronounce transfer of the electron density to the surface in each case. However, the corresponding variation of the partial charge of the octahedral ions (electron density transfer indicated by an arrows in Fig. 2), adjacent to the potassium differs
177

NOEA 2011
Zakopane 4-7 September 2011
for the investigated oxides. It was calculated as -0.09, -0.02 and -0.13 for Co3O4, CoA12O4, and MgCo2O4, respectively. Most pronounced changes in partial charge were observed for Co011 presented in Co3O4, and MgCo2O4. Al octahedral ions presented in CoA12O4 are weakly affected by an electron transfer. The obtained results indicate that the prime deN2O active sites can be identified with the octahedral Co3+ ions, whereas the tetrahedral Co2+ ions alone are much less active, however they play a role of beneficial modifiers for catalytic performance of octahedral Co3+.
Figure 1. TPRS profiles forMgAl2O4, MgCo2O4, CoAl2O4 and for Co 3O4 catalysts
Figure 2. Perspective view of potassium adsorbed on the (J00) plane of cobalt spinel.
1. S.-H. Wei, S. B. Zhang, Phys. Rev. B 63 (2001) 045112
2. F. Zasada, P. Stelmachowski, G. Maniak, J.-F. Paul, A. Kotarba, Z. Sojka, Catal. Lett. 127 (2009) 126
3. L. Obalovd, G. Maniak, K. Kardskovi, F. Kovanda, A. Kotarba, Catal. Commun. 12 (2011) 1055
4. P. Stelmachowski, G. Maniak, A. Kotarba, Z. Sojka, Catal. Commun. 10 (2009) 1062
5. J. J. Hafner, J. Comput. Chem. 29 (2008) 2046
178

NOEA20I1
Zakopane 4-7 September 2011
PS26
##### The use of DESONOX type catalysts to remove nitrogen oxides during coal combustion
##### A. MARCEWICZ-KUBA1
1 Zakład Chemii Środowiskowej, Wydział Chemii, Uniwersytet Marii Curie-Skłodowskiej,
20-031 Lublin Pi. M.C.Skłodowskiej 3
The aim of this study was to determine the effect of a DESONOX type catalyst to reduce emissions of harmful gases such as SO2, CO2 and NOx evolved during combustion of coal with :Bogdanka” mines.
To coal, the catalyst was added at a ratio of 1:1000 and 1:500. Then weighed sample weighing about lg, on an analytical balance to the nearest 0.1 mg. Samples of coal and coal with the catalyst addition burned in a quartz, reactor at the temperature of 1273 K. Each sample of coal and coal with the catalyst at various concentrations was burned several times. The exhaust gases were analyzed by gas analyzer IMR 3000. The analyzer measures the concentration level of O2, CO, CO2, SO2 and NOx. Data from the analyzer were transmitted „on line" to the computer. The degree of reduction in emissions of SO2, CO2, NOx in the flue gas are calculated on the basis of the average concentration of these gases compared with the base, pure coal.
Addition of catalyst DESONOX type to coal in an amount from 0.1 to 0.2 wt. % causes significant reduction of SO2 ,CO2 and NOx in waste gases generated during combustion of coal samples. Reduction of sulfur dioxide is from 26 to 59 %, carbon dioxide from 27 to 37 % and nitrogen oxides from 25 to 40%.
The DESONOX type catalyst changes the combustion process and increases calorie burning fuel by better burning, also reduces the amount of tar evolved during combustion of coal.
1. The DESONOX type catalyst concentration in coal in an amount from 0.1 to 0.2 wt. % reduces the concentration of SO2, CO2 and NOx in the flue gas.
2. With the increase in the amount of catalyst in the coal increases the degree of reduction of harmful gases evolved during combustion of coal samples.
3. Almost twice the effect of a decrease of sulfur dioxide, carbon and nitrogen oxides in the exhaust gas was observed at a ratio of 1:500 the DESONOX type catalyst to coal, that is 0.2 wt. % catalyst in the coal.
4. Coal with the addition of the DESONOX type catalyst bums more and the amount of more evolved tar is less, which means that the ratio of CO2 to the combustion time of coal samples modified as follows: clean coal - 2.75, with the addition of a DESONOX typecatalyst as 1:1000 - 2.04 and for the ratio of 1:500 - 1.98. This means that the concentration of the tar in the gas phase decreased in the first case, declined by 26 % in the second case about 28%.
179

NOEA2011
Zakopane 4-7 September 2011
PS29
##### Multi-step TPSR/QMS technique to study kinetics of NOx SR with ammonia
##### D. Me CLYMONT1,.!. OCHOŃSKA23, S. KOŁACZKOWSKI1, J. LOJEWSKA3
1 Department of Chemical Engineering, University of Bath,
Claverton Down, Bath BA2 7AY, UK
Institute of Chemical Engineering of the Polish Academy of Sciences,
5 Bałtycka St., 44-100 Gliwice, Poland
Faculty of Chemistry, Jagiellonian University, 3 Ingardena St., 30-060 Krakow, Poland
The context of the study is connected with the renewable sources of energy from biomass gasification (e.g. forestry residue, farming residue, municipal waste), to obtain biogas (H2, CO, CO2, N2, HCs) in gas engines. Gas engines (turbines) producing electricity or hot water provide energy at a local level. A major challenge is to develop appropriate catalytic technology for the treatment of exhaust gases (from the engine), to meet the new European Waste Incineration Directive (WID) for this type of a process. The problem of the exhaust gases installation lies in their immense size, ammonia slip, thermal deactivation (hot spots) and catalyst based on nobel metals. The remedy can be the application of the so called structured reactors based on metallic short channel structures of enhanced mass and heat transport [ 1 ] that are able to considerably shorten the reactor length. The application of such structures is entirely dependent on the development of new, highly-active catalysts with an increased conversion adjusted to high transport properties and also the methods of catalyst layering on the metallic surface. In line with the requirements stated by the structured reactors and the NH3-SCR process seem the copper-exchanged zeolites, which are known for their remarkable activity both in in the nitrogen oxides reduction and also in direct NO decomposition [3,4],
This work focuses on the optimization of the Catlab system equipped with tubular reactor and QMS for kinetic studies of NOx selective reduction with ammonia in the presence of oxygen. The equipment enables the multislep TPSR reactions including reduction, oxidation and desorption which used in a sequence provide the information on the active centres for the process. In this study. A real challenge is a proper calibration of the QMS detector for this kind of purposes. For this study the Cu2+-Y zeolite was prepared by exchanging the steamed form of NH4+-Y zeolite (LZY-82, Linde of Si/Ali™, = 4.5) by three­fold ion exchange from aqueous solution of Cu(NO3)2 at 85°C.The sheets of kanthal steal were used as the catalyst carriers. As a reference the ZSM-5 zeolite was also tested. The catalyst was deposited on the surface of the precalcined (1000°C) and washcoated (A12O3 or TiO2) surface of the carriers by impregnation. Both forms of the zeolite catalyst: powder and deposited one were subjected to further analyses. According to the results the most abandoned reactive intermediates during the reaction is oxygen and ammonia and reaction proceed through Rideal-Eley mechanism on Cu* centres on zeolite cavities
[ 1 ] A. Kołodziej, J. Lojewska, Mass transfer for woven and knitted wire gauze substrates: Experiments and modeling,Catal. Today 147S (2009) S120—S124
1. P. Jodłowski, J. Ochońska, D. McClymont, B. Gil, T. Łojewski, A. Kołodziej, S. Kołaczkowski, J. Lojewska,Modelling of structured reactor based on wire gauzes and zeolite catalyst for ammonia reduction of NOx from biogas turbine, submitted to Catalysis Today ((NOEQ 2011)
2. P. Pietrzyk, B. Gil, Z. Sojka, Catal. Today 126 (2007) 103-111
3. K. Sun, H. Xia, Z. Feng, R. San ten, E. Hensen, C. Li, J. Catal. 254 (2008) 383
181

NOEA2011
Zakopane 4-7 September 2011
PS30
##### N2O formation during lean NOX reduction by hydrocarbons over a conventional DOC
##### D. MRAĆEK1, Ś. BARTOVA1, F. PLAT1, P. KOCI1*, M. MAREK1
1 Department of Chemical Engineering, Institute of Chemical Technology,
Prague, Technicka 5, CZ 166 28 Praha, Czech Republic
Corresponding author, e-mail: petr.koci@vscht.cz, http://www.vscht.cz/monolith
Diesel oxidation catalyst (DOC) is utilized for the oxidation of CO and unbumed hydrocarbons (HC) in the diesel exhaust gas. The DOC is also able to reduce a part of nitrogen oxides (NOX) by so-called lean NOx reduction by hydrocarbons (HC-SCR) under excess of oxygen. However, a major by-product of this lean NOX reduction is N2O - a strong green-house gas (GWP=320). Even if the emitted N2O concentrations are low and the contribution of automobiles to global N2O emissions is not major, it is expected that it will be included in future automotive emission regulations.
Experiments were carried out with an industrial DOC in nearly isothermal lab mini-reactor containing three identical monolith samples in series. The inlet gas mixture was prepared online from the individual synthetic gases (CO, C3H6, O2, NO, NO2, CO2, H2O and N2) [1], The experimental series consisted of the ligh-off experiments performed within temperature range 80-400°C (2°C/min). The inlet gas composition was systematically varied to evaluate the effects of NOX, C3H6, O2 and CO concentration as well as the inlet NO2/NOX ratio. The space velocity was 35 000 h'1.
A set of experiments with different inlet concentrations of individual components was performed and the results were obtained by comparing them. The light-off curves of reducing agents (CO and CjHj) were analyzed to evaluate model reaction kinetic parameters (cf. Fig. 1). These effects were observed either in presence of both components, or separately without influence of their interaction. The oxidation of CO ignites below 150 °C, while C3H6 is oxidized more slowly and exhibits light-off at somewhat higher temperature (150-200 °C).
A typical evolution of the outlet NOX, NO2 and N2O concentrations during a slow temperature ramp is shown in Fig. 2. At low temperatures, the NO oxidation to NO2 is inhibited by the presence of CO and C3H6. This inhibition diminishes above the CO and C3H6 oxidation light-off and the production of NO2 increases. It can be seen that a part of NOX is reduced during the C3H6 light-off. After reaching the maximum level of NOX reduction (200 °C), the outlet concentration of nitrogen oxides begin to increase again and the NOX reduction conversion gradually decreases to zero. This is caused by a sharply increasing rale of C3H6+O2 reaction that competes with the NOX reduction. The NOX reduction curve correlates well with the N2O formation curve, indicating that N2O is a major product of this lean NOX reduction by C3H6 over noble metal sites.
The situation with a higher propene concentration is displayed in Fig. 3. It can be seen that higher C3H6 concentration leads to a higher NOX conversion. The selectivity towards N2O decreases only slightly and remains still very high. Fig. 4 shows a case, when CO is present in a higher concentration. CO exhibits a strong inhibition effect on the light-off.
183

NOEA2011
Zakopane 4-7 September 2011
184

NOEA2011
Zakopane 4-7 September 2011
Figure 4. Dependence of outlet concentrations of NO, NO2 and N2O on temperature, inlet: C3H6 = 200 ppm, CO = 1500 ppm
The experimental results show that the lean NO, reduction takes place around the light-off of reducing agents, however only when C3H« is present (pure CO exhibits negligible lean NO, reduction activity). At low C3H« concentrations, almost all NO, reduction leads to N2O. Increase of the inlet C3H6 concentration improves NO, conversion and slightly also the selectivity towards desired product N2. Decreasing inlet 62 concentration in the inlet gas also enhances NO, reduction, but to a smaller extent
NO, adsorption was observed in the same temperature range as the NO, reduction, with a significant competition between NO, and CO adsorption (CO disables the NO, adsorption below the light-off temperature).
185

NOEA 2011
Zakopane 4-7 September 2011
[ 1 ] http://www.vscht.cz/monolith
D. Kryl, P. Koći, M. Kubfćek, M. T. Marek, T. Maunula, M.
Ind. Eng. Chem Res. 44 (2005) 9524
Hiirkónen,

NOEA 2011
Zakopane 4-7 September 2011
PS31
#### Effect of O2, SO2 and H2O on NO decomposition over Ni-Cr-Fe oxide catalysts
#### J. DUTKIEWICZ1, S. .JANIGA1,1. NAZARCZUK1, M. KOZICKI1, P. KORNELAK1, M. NAJBAR*
Faculty of Chemistry, Jagiellonian University, 3 Ingardena St., 30-060 Kraków, Poland
An anatase-supported V-O-W catalysts are commonly used to abate NOX emission from stationary sources by their reduction with ammonia. However, ammonia is corrosive, relatively expensive, and poisoning.
NO is the main component of NOX in off-gases of stationary sources of emission. It is formed in endothermic N2 oxidation and shows high thermodynamic instability. Thus, a direct decomposition of NO could be the best method of NO removal.
Recently, Reichert et al. 11-2] performed an interesting investigation of the reaction of NOX and soot on Fe2O3 catalyst in excess of O2. They have postulated, the direct NO decomposition on carbon activated by oxygen species formed on Fe2O3. Pirogova et al. [3] investigated activity of chromites with a spinel structure in NO decomposition in the reducer presence.
Figure I. Temperature dependence of the CN(> and the SN2 in the direct NO decomposition on a powdered Ni-Cr-Fe oxide catalyst scraped off a surface of a acid-resistant IH18N9T/4541 steel tube, where it was formed in the course of a few thermal treatments composed of the heating to 84ff’C and next annealing at this temperature for 4 h; catalyst-0.200g, reaction gas-2()()ppmNO/He; GHSV= 7000h'.
We have investigated the activity of the Ni-Cr-Fe oxide catalysts in the direct NO decomposition (200ppm-2%NO): i/ in the absence of any other reactants, ii/ in the presence of 5-7.4% of O2, iii/ in the presence of 7.4% of O2 and 200-1600ppm SO2 iv/ in the presence of 7.4% of O2, 200ppm SO2 and 20-40ppm H2O.
187

NOEA2011
Zakopane 4-7 September 2011
That catalyst was formed on surfaces of the austenitic acid-resistant supports (tubes, sheets of foils and monoliths) as a result of their thermo-programmed heating and next annealing in oxygen-conlaining atmosphere. Catalytic tests were performed either in a tubular quartz reactor on line with H-P 5890 GC equipped with Molsieve 5A column and TC detector (1 and 2%NO/He) or in an u-tube flow reactor (160-1000ppm NO/He) on line with Agilent Technologies GC-MS equipped with a capillary DB-1 column.
In Fig. 1 temperature dependences of the NO conversion (CN0) and selectivity to N2 (SN2) in the direct NO decomposition (200ppmNO/He, GHSV= 7000h ') on a powdered Ni-Cr-Fe oxide catalyst (0.200g), are presented. The catalyst was obtained on the surface of the acid-resistant 1H18N9T/1.4541 steel tube (wall thickness ca. I mm) in the course of thermal treatment composed of the heating to 840°C in air and next annealing at this temperature for 4 h. It was placed on a quartz crust in the u-tube flow rector and was activated at 600°C in helium for Ih prior the activity test. The activity and selectivity to N2 were determined from the results of the periodical analyses of the effluent gas.
In the whole temperature range the SN2 is close to 100%, whereas CN0 achieves 100% at 400°C.
The results (not shown here) of the analogous experiment performed with the use of reaction gas composed of 200ppm NO, 7.4% O2 and helium balance show an increase of the NO conversion to nearly 100% in a 150-350°C temperature range and a slight decrease in the selectivity to N2 at the highest temperatures.
However, the results (not presented here) of the analogous experiment with the use of the reaction gas composed of 200ppm NO, 7.4% O2 and 200ppm SO2 and helium balance reveal SO2 addition does not cause distinct changes in CN0 and leads to some increase of the SN2 at the highest temperatures
Publication co-financed by the European Regional Development Fund under the Innovate Economy Operational Programme 2007-2013, POIG.01.01.02-12-112/09 project.
[ 1 ] D. Reichert, H. Bockhom, S. Kureti, Appl. Catal. B: Environ. 80 (2008) 248
1. D. Reichert, T. Finke, N. Atanassova, H. Bockhom, S. Kureti, Appl. Catal. B: Environ. 84 (2008) 803
2. G. N. Pirogova, N. M. Panich, R. I. Korosteleva, Yu. V. Voronin and N. N. Popova, Russian Chemical Bulletin, International Edition, 50 (2001) 2377
188

NOEA2011
Zakopane 4-7 September 2011
PS32
##### NOX uptake and storage properties of BaOx/Pt(lll) model catalyst: influence of Ba coverage, surface morphology and stoichiometry
##### E. ÓZENSOY1*, E. VOVK1, E. EMMEZ1
1 Department of Chemistry, Bilkent University, Ankara 06800, Turkey,
Corresponding author: ozensoy@fen.bilkent.edu.tr
Atomically ordered, BaO ultrathin films were synthesized on a planar Pt(l 11) single crystal to obtain a reverse model catalyst for NO, Storage Reduction catalytic processes. The structure of the BaO nano-domains and their relevance to NOX catalytic chemistry was investigated under UHV conditions using a combination of XPS, LEED and TPD techniques.
NOX storage reduction or Lean NOX technology, which is commonly referred as NSR or LNT, is a promising after treatment technology for lean-bum engines. However there is still very limited knowledge regarding the catalytic processes that occur during the NSR systems at the molecular scale. [1-4] In order to address some of the important fundamental surface science issues relevant to the molecular understanding of the NOX storage process on the NSR catalysts, various BaOx/Pt(ll I) reverse model catalyst were synthesized and their interactions with NO2(g) were investigated as function of the surface coverage, morphology and stoichiometry of the BaOx overlayer on the Pt(lll) single crystal substrate.
Experiments were performed in a custom-design multi-technique ultra high vacuum (UHV) surface analysis chamber which is equipped with a X-ray photoelectron spectrometer (XPS),a quadruple mass spectrometer (QMS) for temperature programmed desorption (TPD) analysis, reverse-view low energy electron diffraction (LEED) optics, metal evaporators for thin-film deposition and high-precision gas dozers for adsorption studies. The typical base pressure of the UHV system was 2 x IO10 Torr Pt (111) single crystal substrate (Mateck GmbH) was mounted on the sample holder using Ta wires. Temperature of the sample was measured using a K-type thermocouple directly spot-welded on the Pt (111) crystal. The sample temperature can be varied within 100 K - 1100 K. Before the film growth, Pt (111) surface was cleaned by successive cycles of Ar+ ion sputtering and annealing in vacuum al 1073 K. BaOx films were grown using two different synthetic protocols which included evaporation of Ba from a BaAl(s) evaporation source followed by two different oxidation recipes.
BaO/Pt( 111) (LEED) and decreasing NOX desorption maxima with decreasing Ba coverage after NO2 adsorption on BaO/Pt( 111) (TPD).
BaOx/Pl(lll) inverse model catalysts were prepared by either: i) evaporation of metallic Ba on a thick multi-layer of solid NO2 on Pt (111) at 100 K followed by annealing in vacuum at 1078 K or ii) evaporation of metallic Ba on a thick multi-layer of solid NO2 on Pt (111) at 100 K followed by oxidation in 1 x 1 O'7 Torr of O2(g) at 1078 K. These two preparation procedures were repeated for various Ba surface coverages ranging from sub-monolayer BaOx overlayers to multi-layer (thick) BaO films.
189

NOEA2011
Zakopane 4-7 September 2011
Figure 1. NO2 and NO3 formation on (thick) BaO/Pt(lll) (XPS), crystal structure of different ordered overlayers for (thin)
Various atomically ordered BaO„/Pt(lll) overlayers were detected in the LEED experiments for low Ba surface coverages while thick films led to amorphous disordered overlayers. Our XPS experiments revealed indications for the presence of BaO2 for the model catalysts which were prepared by oxidation in the O2(g) environment (procedure (if) while model catalysts prepared with vacuum annealing (procedure (ii)) resulted in BaOx (x < 1) stoichiometry. These two different types of overlayer stoichiometries also seem to have different surface morphologies for multi-layer (thick) Ba overlayers. This argument is supported by the TPD experiments, which showed the evolution of N2(g) species after NO2(g) exposure on (thick) BaO2/Pt(l 11) surface implying the presence of exposed (uncovered) Pt sites which catalyze the activation of the N-0 linkages and formation of atomic N(ads) species which recombinatively desorb as N2(g).
On the other hand, (thick) BaO/Pt( 111) surfaces do not reveal a well-defined N2(g) desorption signal due to the complete wetting of the Pt( 111) substrate with the BaO overlayer. Furthermore, influence of the Pt sites on the N-0 bond activation becomes even more evident for sub-monolayer BaO or BaO2 overlayers on Pt(lll). As the surface coverage of Ba decreases, number of exposed Pt sites increases and these exposed Pt sites function as active reduction centers for the surface NO, species (which are in the form of nitrites and nitrates based on our XPS results) and efficiently facilitate decomposition of the adsorbed NOX species at lower temperatures
1. E. Ozensoy, J. Szanyi, C. H. F. Peden, J. Catal. 243 (2006) 149
2. E. Ozensoy, J. Szanyi, C. H. F. Peden, J. Phys. Chem. B 110 (2006) 8025
3. S. M. Andonova, G. S. Senturk, E. Ozensoy, J. Phys. Chem. C 114 (2010) 17003
4. E. Vovk, E. Emmez, E. Ozensoy in preparation
190

NOEA20II
Zakopane 4-7 September 2011
PS33
##### Selective Catalytic Reduction of NOX by C2H5OH over Ag/AhOa/cordierite
##### N. POPOVYCH1, P. KIRIENKO1, S. SOLOVIEV1
1 L. V.Pisarzhevsky Institute of Physical Chemistry of the NAS of Ukraine,
31 Prosp. Nauky, 03028 Kyiv, Ukraine, nataliepopovich@mail.ru
The abatement of nitrogen oxides (NOX) emitted by mobile and stationary sources requires effective and durable SCR catalytic system that works in oxygen-rich environments. Among the various catalysts proposed for SCR with hydrocarbon or oxygenated organic reductants an alumina-supported silver was found to be the most active and potential catalytic system and has received considerable attention [1], The advantage of oxygenated compounds over hydrocarbons is their higher reactivity; moreover some oxygenated compounds (e.g. ethanol) are environmentally relatively benign and can be used as components of vehicle fuel.
Structured catalysts are widely used for atmospheric emissions purification in practice but there are no research data about supported Ag/Al2O3 in literature. Thus study and design of structured catalysts for SCR NOX are an important challenge.
Ceramic block matrices with a honeycomb structure made from synthetic cordierite (2Al2O3-2MgO-5SiO2) were used as a catalyst support. The catalyst surface was formed by coating with y-Al2O3 (confirmed by XRD) from aqueous solution of KOH+aluminium swarf and by incipient wetness impregnation with an AgNO3 aqueous solution. Then samples were dried in the air and calcined at 750°C. The silver and alumina loadings on the cordierite are reported in wt. %. The catalytic activity was characterized by the NO conversion (chemiluminescent detector) in the reaction mixture: 500ppm NO + 0.2%C2H5OH + 5%O2 in He (GHSV = 20 000 h1). The specific surface area was obtained by the thermal desorption of nitrogen (for samples after SCR). UV-Vis diffuse reflectance spectra (DRS) were recorded under ambient conditions on a Specord M40 with a standard diffuse reflectance unit (for samples after SCR). The spectra reported here were obtained by subtraction of the support spectrum to that of the Ag/Al2O3 supported samples.
The catalytic results for samples with different content of Ag (Tab.l) show that there is almost complete conversion of NO for 0,1-0,5% Ag. It is clear from our results that not only silver content in the sample effects on the activity of structured silver-alumina catalysts, but also content of alumina. One can see that both over a composition 0.3%Ag/48%Al2O3/cordierite and over a 0.5%Ag/48%Al2O3/cordierite complete conversion of NO is achieved in the temperature range 300-450 °C but NO conversion over a 0.3%Ag/27%Al2O3/cordicrile is 95% al 340-360 °C and over a 0.5%Ag/27%Al2O3/cordierite is 80% at 300-330 °C. Complete conversion of NO over the catalyst 0.1%Ag/27%Al2O3/cordierite is observed for temperatures as high as 390-410 °C whereas for the sample 0.1%Ag/48%Al2O3/cordierite this range is much wider (380-440 °C) even in comparison with sample which contains three times more silver but only 27% y-AI2O3. Over the samples contained only alumina (N»2,7) temperature of 50% NO conversion for 48%Al2O3/cordierite on 70 °C lower than for supported 27%/Al2O3.
It is worth noting that the deposition of silver up to 0,5% does not lead to a decrease in specific surface and in some cases (catalysts 3, 8 and 9) even increases specific surface of supported catalysts apparently due to highly dispersed distribution of silver on alumina surface. Thus, as clear from data in Tab.l, the most active structured silver-alumina catalysts are that with higher specific surface area (in terms of the same content of y-Al2O3 in the catalyst), and aren’t that with higher silver content. Probably the introduction of more than 0.5% of silver leads to its encapsulation in the depths of the alumina matrix.
191

NOEA 2011
Zakopane 4-7 September 2011
Tab. I. Catalytic activity and specific surface of cordierite-supported catalysts
N»	Catalysts	NO Conversion, % /At, °C	S. m2/g
1	l%Ag	0	1.5
2	27%A12O3	-50/450-500	24
3	0.1%Ag/27%Al2O3	-98/390-410	26
4	0.3%Ag/27%AI2O3	-95/340-360	22
5	0.5%Ag/27%Al2O3	-80/300-330	20
6	l%Ag/27%Al2O3	-35/290-340	22
7	48%A12O3	-50/380-500	38
8	0.1 %Ag/48%Al2O3	-100/380-440	44
9	().3%Ag/48%Al2O3	-100/320-440	41
10	().5%Ag/48%Al2O3	-100/320-440	38
11	1 %Ag/48%Al2O3	-100/300-330	38
12	1.5%Ag/48%Al2O3	-75/295-365	37
13	2%Ag/48%Al2O3	-70/270-290	37

Results of UV-VIS DRS show (Fig. I) that the greater part of silver is ions of Ag+ (the peaks at 225 and 260 nm) [2,3]. The peak near 450 nm could be assigned to metallic silver particles. Al high silver loading in the catalysts the peak near 450 nm is higher therefore the quantity of silver nanoparticles which are responsible for the total oxidation of the ethanol by oxygen is greater |4|. The increased content of alumina contributes to increase of silver dispersion on alumina surface and prevents its agglomeration in the process of catalyst preparation and at reaction conditions.
Figure I. Diffuse reflectance UV-VIS spectra of samples (numbers of curves are identical to numbers in Table)
11] S. Kameoka, Y.Ukisu. T.Miyadera, Phys Chem Chem Phys. 2 (2000) 367
1. N. Bogdanchikova, F.C. Meunier, M. Avalos-Borj, et al.. Appl. Catal., B: Environ 36 (2002) 287
2. A. Musi, P. Massiani, I). Brouri, et al., Catal Lett 128 (2009) 25
3. M.C.Kung, H.H.Kung, Top. Catal. 10 (2000) 21
192

NOEA20I1
Zakopane 4-7 September 2011
PS34
##### Study of the interaction of NOX and NH3 with the surface of copper and nickel catalysts supported on ceria-zirconia by FT-IR spectroscopy
##### M. RADLIK13 A. ŁAMACZ1, A. KRZTOŃ1, W. TUREK2
1 Polish Academy of Sciences, Centre of Polymer and Carbon Materials, Zabrze, Poland
1 Silesian University of Technology,
Department of Physical Chemistry and Technology of Polymers,
Gliwice, Poland
Nitrogen oxides (NO, NO2 and N2O) emitted from stationary boilers and mobile engines contribute to a lot of environmental problems. They are major source of acid rain, photochemical smog, ozone depletion and greenhouse effects [1,21. Several methods have been proposed for NOX removal [3]. One of the most promising and effective is Selective Catalytic Reduction SCR. This technology depends on both catalysts and reductant agent. Typical reductant agent are hydrocarbons, ammonia or urea. Among them ammonia is known to be very selective towards N2 and provides high efficiencies [4]. Various catalysts have been investigated for NH3-SCR deNOx, such as transition metal oxides, zeolite-based catalyst and noble metal catalysts [5]. Catalysts should be stable and active in the interaction with gas phase (containing NOX and NH3). It can be observed by FT-IR spectroscopy in temperature DRIFT cell. This technique give information about the catalyst surface during adsorption NOX or/and NH3 from gases phase and determining the structure of adsorbed species.. The aim of this work is to show structure of adsorbed species on the surface catalysts during deNOx experiments using, temperature DRIFT cell.
The copper and nickel catalysts supported on ceria-zirconia, obtained by wet chemical impregnation with different amount of metal were studied during the interaction with gas phase, containing NOX and/or ammonia.
We observed nitrate ions and different groups, like NHf, NH2 for adsorbed NOX and NH3 species respectively, similar to others work [6, 7], Among it we observed interaction NOX and ammonia with catalysts surface, allows to exclude no active catalysts and explains some details of mechanism of the ammonia in selective catalytic reduction.
[ 1 ] Zhichun Si, Duan Weng, Xiaodong Wu, Jia Li, Guo Li Journal of Catalysis 27,43-51,2010
1. Hideharu Iwakuni, Yusuke Shinmyou, Hiroshi Yano, Hiroshige Matsumoto, Tatsumi Ishihara Applied Catalysis B: Environmental 74, 299-306, 2007
2. Zhiming Liu and Seong Ihl Woo Catalysis Reviews, 48,43-89,2006
3. A. Boyanoa, MJ. Lazaroa, C. Cristiani, F.J. Maldonado-Hodarc, P. Forzatti, R. Molinera Chemical Engineering Journal 149, 173-182,2009
4. Zhiming Liu and Seong Ihl Woo Catalysis Reviews, 48,43-89,2006
5. Małgorzata Adamowska, Se'bastion Muller, Patrick Da Costa, Andrzej Krzton, Philippe Burg, Applied Catalysis B: Environmental 74,278-289, 2007
6. Maria Casapu, Oliver Krocher, Max Mehring, Maarten Nachtegaal, Camelia Borca, Messaoud Harfouche, and Daniel Grolimund, J. Phys. Chem. C 114,9791-9801,2010
193

NOEA20I1
Zakopane 4-7 September 2011
PS35
##### Catalytic reduction of NO by CO over FexSiBEA catalysts
##### I. HNAT1,1. KOCEMBA1’, J. RYNKOWSKI1, S. DŹWIGAJ2*
1 Institute of Ecological Chemistry, Technical University of Lodz, Poland
2 Laboratoire de Reactivite de Surface,UPMC, CNRS, UMR 7197, 3 rue Galilee,
94200 Ivry-sur-Seine, France
^Corresponding authors: ireneusz.kocemba@p.lodz.pl, stanislaw.dzwigaj@upmc.fr
Il is well known that iron loaded zeolites are active catalysts of selective catalytic reduction (SCR) of NO by hydrocarbons or ammonia [1,2]. Recently [3,4], we have reported that introduction of iron ions into the zeolite framework by two-step postsynthesis method allows to obtain a material with very good catalytic properties in SCR of NO by ethanol. It has been shown that catalytic activity of FexSiBEA zeolites strongly depends on the nature and state of iron introduced into the zeolite structure.
In the present work this poslsynthesis method is used to obtain FexSiBEA catalysts (x = 0.6, 1.0, 2.0, 4.0 and 10 Fe wt %) with mainly iron present as isolated tetrahedral or octahedral Fe(III) species. The aim of this study is to investigate the influence of nature of iron on catalytic properties of FexSiBEA zeolites in SCR of NO by CO.
This process, leading to the removal of two toxic reactants, is environmentally very important reaction.
2CO + 2 NO = 2CO2 + N2	(I)
The aim of this work is investigation of the catalytic activity of FeSiBEA in the NO reduction with CO
FexSiBEA catalysts (x = 0.3 - 10 Fe wt.%) were prepared by the two-step postsynthesis method described earlier [5]. As prepared FexSiBEA catalysts were calcined in air at 500 ° C for 3 h and reduced by CO for 0.5 h at 700 0 C. The catalysts were characterized by different physicochemical methods: XRD, SEM, diffuse reflectance (DR) UV-VIS and TPR-CO. The catalytic tests were carried out using Temperature Programmed Surface Reaction method (TPSR) in a fixed-bed reactor (mass of the catalyst - 200 mg), in the temperature range 25 - 500 °C, with a linear increase in temperature (10°C /min). Gas mixture: 1 vol.% CO + I vol.% NO + He (balance) and total GHSV 4800 h'1 was used. The changes in CO and N2 concentration in the outlet of gas mixture were analyzed by Fuji IR Gas Analyzer and GC chromatography using a 5A molecular sieves column and TCD detector.
The CO conversion and selectivity to N2 were calculated by the following equations:
CO conversion = ([CO],„ - [CO]„„,) / [CO]jn * 100%	(2)
Selectivity to N2 = [N2 ](Mt / [N2 ],/, * 100%	(3)
where [N2],ft is theoretical concentration of N2 according to reaction (1) calculated from equation:
[N2],„ ='/2([CO],„- [CO]ou1)	(4)
Table 1 shows the temperature of 50% conversion (T50) of CO and selectivity toward N2 for FexSiBEA containing different Fe content. The CO conversion is relatively low, reaching only ca. 80% at 500 °C for the best catalysts. The different catalytic properties of FexSiBEA may be due to the different nature of iron species. Figure 1 shows CO conversion and the TPR-CO profile of Fei 0 SiBEA sample. A striking feature is the similarity of CO conversion and TPR-CO profiles. It can indicate the correlation between reducibility of catalyst and the mechanism of CO + NO reaction.
195

NOEA 2011
Zakopane 4-7 September 2011
Table 1. The catalytic performance ofFefiiBEA (x = 0.3 -10 Fe wt. %) samples
x (wt. %)	0.3	1.0	2.0	4.0	10
Tso (°C)	430	370	410	414	405
Selectivity* to N2	36	42	37	48	62

' Selectivity at the temperature of 50% conversion (T50) of CO
Fig.l. TPR-CO profile and CO conversion for Fe/^iBEA catalyst
The mechanism of the reaction (1) can be considered as occurring in two stages. In the first, the reduction with CO of (Fe O)SiBEA to (Fe)SjBEA species probably takes place:
(Fe O)$iBEA + CO —» (Fe)siBEA + CO2	(5)
It explains the similar course of TPSR and TPR-CO processes.
In the second one the direct decomposition of NO on the reduced form (Fe)SiBEA occurs, simultaneously restoring (Fe O)siBEA species:
NO + (Fe)SiBEA -» (Fe	O)SiBEA + Vi N2	(6)
The decomposition is efficient as long as the iron species in the reduced form remain. Their oxidation leads to the catalyst deactivation, which is responsible for a low stability of the catalysts under study in the reaction.
1. H.H. Chen, S.C. Shen, X. Chen, S. Kawi, Appl. Catal. B 50 (2004) 37
2. P. Balie, B. Geiger, S. Kureti, Appl. Catal. B 85 (2009) 109
3. J. Janas, J. Gurgul, R.P. Socha, T. Shishido, M. Che, S. Dźwigaj, Appl. Catal. B	91	(2009) 113
4. S. Dźwigaj, J. Janas, T. Machej, M. Che, Catal. Today 119 (2007) 133
5. I. Hnat, I. Kocemba, J. Rynkowski, T. Onfroy, S. Dźwigaj, Catal. Today, 2011	in	press
196

NOEA2011
Zakopane 4-7 September 2011
PS36
##### Preparation and characterization of T1O2 based plasma sprayed catalytic coatings for NOX abatement
##### V. SNAPKAUSKIENE1, V. VALINCIUS1
1 Lithuanian Energy Institute, Plasma Processing Laboratory,
Breslaujos 3, LT-3035 Kaunas, Lithuania, e-mail: vilma@mail.lei.lt
Il is initial part of a systematic study on the preparation and catalytic performance on metal oxide catalysts for the CO + NOX redaction. As our previous works have shown, catalytic coatings, deposited by plasma spray technology from active component CuO, reduce effectively the amount of CO in the exhaust gas (Snapkauskiene et al. [1]). The aim of further work is to select catalyst for NOK redaction. For this reason TiO2 and Ni powder were incorporated additionally and in the first instance the system active layer-substrate was analysed to define the phase, morphology and roughness of new composition coatings.
The catalytic coatings 90 pm of thickness were prepared by plasma spraying (power of plasma torch 35 kW, arc current 165 A, enthalpy 955 kJ/kg, reactor chamber diameter 10 mm, spraying distance 120 mm, plasma forming gas - air) on heat-resistant foils of FeCrAl type as a support. The support was covered with an active layer consisting of various mixture of 10-15 wt.% TiO2 (anatase, 325 mesh; Aldrich), 10 wt.% Cu (325 mesh; Alfa Aesar) and 10 wt.% Ni (400 mesh; Alfa Aesar) with aluminium hydroxide in balance. All coatings were healed in air at 560°C for 1.5 h.
The surface morphology and microstructure of the obtained samples was studied by scanning electron microscope (ESEM) Quanta 200 FEG (FE1 Ltd, Eindhoven, Netherlands), coupled with an energy-dispersive X-ray microanalysis (EDX) spectrometer Quantax 200 (Broker, Germany). The weight percent concentrations of individual surface precipitates have been calculated automatically by EDX software. The analysis of images was done with the ImageJ software. The XRD patterns of the synthesized and healed coatings were recorded with a conventional Bragg-Brentano geometry (0 - 20 scans) on a DRON-6 automated diffractometer equipped with a secondary graphite monochromator. Cu Ka radiation (k = 1.541838 A) was used as a primary beam. The patterns were recorded from 5 to 70° 20 in steps of 0.02° 20, with the measuring time of 0.5 s per step. The surface roughness of coating layers was measured by surface analyzer-profilometer Hommel Tester T500 (Germany).
Analysis of SEM views of plasma sprayed coatings showed, that all coatings are characterized by homogeneous and dense structure (Fig. 1). The distribution of pores and voids is quite homogeneous, but also irregularly agglomerated metal oxide layers are formed. The morphology of all samples is more similar than different despite of the different composition of started powder. After the coatings heating at the temperature of 560°C, a positive phenomenon was observed when the surface of voids in active layer has been on the increase. EDX mapping images showed quite even distribution of active components in the washcoat.
As it can be seen in Fig. 1, the roughness profiles of the as-sprayed surfaces obtained by traversing across the test surfaces using a profilometer are rather similar independent of whether the surface is fresh or healed. By the data presented the main parameter of surface roughness Ra of metal oxide coatings varies from 3.4 pm to 5.2 pm. The less roughness is typical for coatings with higher content of titania. The maximum roughness, i.e. the difference between the roughness maximum depth and maximum height, varies from 25 pm (15 wt.% TiO2) to 43 pm (15 wt.% TiO2/10 wt.% Cu/10 wt.% Ni). This parameter depends significantly not only on the number of coating layers, but also on the jet outflow regime, the flow rale of the plasma-forming gas, the applied power or the average bulk temperature, and the spraying distance (Prancvicius at al. [2]).
Qualitative EDX analyses are in agreement with XRD results. The XRD patterns confirmed a titanium dioxide phase of all tasted simples and showed presence of two modifications - rutile and anatase with tetragonal crystal systems. Also results on XRD analysis of catalytic coalings show the
197

NOEA2011
Zakopane 4-7 September 2011
domination of pure copper and copper oxide Cu2O as well as pure nickel and nickel oxide NiO, respectively. Heated simples do not show important differences in diffraction peaks.
Figure 1. SEM micrograph (above) and surface profile (down) of fresh and heated coatings
According to obtained results all new coatings are suitable for the analysis of catalytic processes. The multitubular catalytic monolithic reactors were manufactured of these coatings on the purpose to test it for the NOX redaction in our improved experimental equipment with a reactant mixture containing 2000 ppm of NO, 5% of CO, 21 % of O2 and nitrogen as balance.
198

NOEA2011
Zakopane 4-7 September 2011
Postdoctoral fellowship is being funded by European Union Structural Funds project "Postdoctoral Fellowship Implementation in Lithuania
[ 1 ] V. Snapkauskiene, et al., Catal. Today (2011), doi: 10.1016/j.cattod.2011.02.023
L. PraneviCius, L.L PraneviCius, P. Valatkevicius, V. ValinCius. Surf. Coat. Technol. 123 (2000) 122
too

NOEA20I1
Zakopane 4-7 September 2011
PS37
##### MgF2-MgO system as a potential support for NiO catalysts for NOX reduction by propene
##### M. ZIELIŃSKI1’, I. TOMSKA-FORALEWSKA1, M. PIETROWSKI1, M. WOJCIECHOWSKA1
1 Faculty of Chemistry, Adam Mickiewicz University, Grunwaldzka 6, 60-780 Poznań, Poland
*e-mail: mardok@amu.edu.pl
Nitric oxides (NOX) are the most commonly encountered air pollutants, causing acid rain and climate changes. These pollutants are emitted into the atmosphere mainly from oil/coal-fired furnaces and automobile exhaust. In recent years, much attention has been focused on the removal of these air pollutants because of the pressure of stricter regulations concerning the environment protection [1,2],
Selective catalytic reduction of NO by hydrocarbons (HC-SCR) is a potential method to remove NO from exhaust gases. The performance of zeolites, metallic and oxide systems in this process has been widely tested. In respect to vehicles, a well-established technology for NOX, CO and hydrocarbons emissions control is based on the three-way catalyst (TWC). In a conventional three-way catalytic converter, noble metals such as Pl, Pd (both effective in oxidizing CO and hydrocarbons) and Rh (responsible for NOX reduction) are commonly used. Due to the high costs of precious metals, considerable efforts have been made to develop catalysis using of cheaper transition metals and their oxides. One of the most active metal oxide in the process of deNOx is NiO. The NiO/support catalysts exhibit high activity both in NO reduction by CO under stoichiometric conditions in the absence as well as in the presence of oxygen and in NO reduction by hydrocarbons.
This paper reports NiO/MgF2-MgO activity in the NO+C3H6+O2 reaction depending on properties of the support. The MgF2-MgO system is tested as a potential support of nickel oxide catalysts in the NO+C3H6+O2 reaction depending on the MgO/MgF2 ratio in the support and the reaction conditions. The study was performed at temperatures ranging from 250 to 475°C in the reducing, oxidizing and stoichiometric conditions. The activity of the nickel oxide catalysts was compared to NiO/MgF2 and NiO/MgO.
Synthesis of supports
The MgF2 and MgF2-MgO supports with different MgO content were obtained in the reaction of basic magnesium carbonate (4MgCO3Mg(OH)2-5H2O) powder with controlled amounts of aqueous solution of hydrofluoride. The amount of hydrofluoride solution was chosen to ensure 0 , 40, 60 and 100 mol.% of MgF2 in the support. The suspension obtained was evaporated then dried at 80°C for 24h and calcined under the air flow at 400°C for 4h.
Synthesis of nickel catalysts
MgO, MgF2-MgO and MgF2 supports, calcined at 400°C were impregnated with an aqueous solution of nickel(II)-nitrale hexahydrate in the amount ensuring 1 wt.% nickel in the catalysts. The samples, were dried at 110°C for 24h then calcined at 400°C for 4h in air.
Supports and catalysts characterization
The supports and the catalysts were characterized by the low-temperature adsorption of nitrogen, X-ray diffraction, thermo-gravimetric analysis, temperature-programmed reduction.
Catalytic lest
The reaction of NO + C3H6 + O2 was performed by a continuous method. The reacting gases (1 vol.% of NO in He, I voi.% of propene in He and 5 vol.% of O2 in He) were flown al the total flow rate of the reaction gases 50cm3/min through a quartz reactor filled with O.lg of the catalyst. In order to remove water, before reaction catalysts were activated in helium at 400°C during Ih. The reaction was run at temperature range 250-475°C. The activities of the catalysts were determined in different reaction conditions described by the parameter R defined by Tanaka et al., [3]: Rcl reducing conditions, R=1 stoichiometric and R>l oxidizing. The reaction products were analyzed using Carlo Erba 6000 GC
201

NOEA 2011
Zakopane 4-7 September 2011
equipped with 2m long column filled with 13 X molecular sieves (2/3) and chromosorb 104 (1/3). The catalytic activity was presented as apparent rate - r, (pmolN(//JmolNlh) - calculated for the total Ni content in a catalyst (1 wt.%).
This paper reports the results of a study on the structure of nickel oxide supported on MgF2-MgO of different composition and pure MgF2 and MgO. The activity of the nickel oxide catalysts containing I wt.% Ni supported on MgF2 and MgO were compared with that of the nickel catalyst obtained by impregnation of the other supports - A12O3, SiO2 - Figure I. According to the results the most active were the catalysts supported on MgF2, although with increasing temperature their activity decreased as a result of the competitive propene oxidation reaction. The study was performed at temperatures ranging from 250 to 475°C in the reducing, oxidizing and stoichiometric conditions.
The activity of the NiO/MgF2-MgO catalysts was compared to those of Ni()/MgF2 and NiO/MgO. The highest activities are obtained for the catalysts supported on pure MgF2 especially in the reducing conditions. Mixed system MgF2-MgO gave a support on which nickel revealed much higher activities in NO reduction both in reducing and in oxidizing conditions compare to NiO/MgO catalyst. Figure 2 presents the activity of the nickel catalysts versus the content of MgF2 in the support for different R values. The NiO/MgF2-MgO catalysts were more active in the reducing conditions and their activities increase with increasing of MgF2 content in the mixed MgF2-MgO supports. At an excess of oxygen (oxidizing conditions), their activities decreased.
Figure I. Catalytic activity of NiO phase supported on different supports in NO reduction by propene as a function of temperature (R=0.4)
202

NOEA201I
Zakopane 4-7 September 2011
Figure 2. Catalytic activity of nickel oxide catalysts in the reaction NO+CjH(,+O2 at 375" C for different compositions of the reaction mixture
We thank the Polish Ministry of Scientific Research and Information Technology for financial support under the projects N N204 141339 and N N204 214140.
[11 Worldwide Fuel Charter, Fourth Edition, September 2006
1. Official Journal of the European Union, REGULATION (EC) No 715/2007 OF THE EUROPEAN PARI JAMENT AND OF THE COUNCIL of 20 June 2007
2. T. Tanaka, K. Kokota, N. Isomura, H. Doi, M. Sugiura, Appl. Catal. B 16 (1998) 199
203

NOEA2011
Zakopane 4-7 September 2011
PS38
##### Raman spectroscopic studies of the oxide Ni-Fe-Cr catalysts for NO decomposition
##### A. WESEŁUCHA-BIRCZYŃSKA1, M. KOZICKI1, M. NAJBAR1
1 Jagiellonian University, Faculty of Chemistry, 3 Ingardena St., 30-060 Kraków, Poland
NOX (NO and NO2) belong to the most dangerous air pollutants. Ammonia is commonly used to remove NOX from off-gases of stationary sources of emission. It is also applied for their removal from Diesel engine exhausts. However, ammonia as a reducer has several drawbacks; it is corrosive, relatively expensive and poisonous. Therefore, there is a great effort to replace ammonia by another reducer or to remove NO by direct decomposition to dinitrogen and dioxygen.
A current paper concerns Raman spectroscopic investigations of oxide phases forming on the surface of acid-resistant steel foil in the course of its oxidation and showing good activity in the direct NO decomposition.
Oxide phases were formed on the acid resistant austenitic steel (1 Hl8N9T/1.4541) tubes and resistant austenitic steel (OH 18N9/1.4301) sheets of foil by thermo-programmed heating from room temperature up to 850 °C in air or in the stream of air or oxygen and then annealing at the final temperature for and 4 hours, respectively. Heating and annealing were performed once or several times to obtain oxide layers of different temperatures. Powder of oxides was scraped from the oxidized tubes. However, oxidized foils were investigated directly in spectrometer.
Raman spectra were collected using Raman Renishaw inVia micro-spectrometer working in confocal mode. Samples were excited with 785 nm laser line of HP NIR diode laser. The laser power was low to ensure that it not destroys sample.
In a figures 1 (a-c) the micrographs of the chosen areas of oxide sample scraped from the tube annealed at 650 °C are presented. Figure Id demonstrates Raman spectra collected from the micro areas marked in the Figures 1 a-c.
A scale grown on the surface of the acid resistance steel tube is composed of a-Fe2O3 [1,2] and spinel phase (Ni,Fe)(Fe,Cr)2O4 [3-6]. The position of the main peak of the spinel phase depends on the content of chromium in tetrahedral positions and content of nickel in octahedral one. It shifts towards higher wavenumbers with the increase of Cr as well as Ni content. The reduced a-Fe^ phase as well as spinel phases are known to be active in NO decomposition. The coexistence of both phases may increase this activity due to strains on the phase boundaries enhancing mobility of the lattice oxygen atoms. Further increase of the activity of the scale may be caused by the formation of Cr/ Fe2O3 solid solution and/or by Ni2+ substitution for Fe2+ and Cr3* substitution for Fe3* in spinel phase.
Raman spectra of the rust on the oxidized foil from OH 18N9/1.4301 sheets resemble those of the powder scraped from 1H18N9T/1.4541 tubes. The most visible difference is the position of the main peak of the spinel phase. This position is closer to that of Fe3O4. It reveals that several oxidation procedures are needed to introduced chromium and/or nickel to magnetite.
205

NOEA2011
Zakopane 4-7 September 2011
1. S.H. Shim.T.S. Duffy, Raman spectroscopy of Fe2O3 to 62 GPa, Am. Mineral., 87 (2001) 318-326
2. MJ. Massey, U. Baier, R. Merlin, W.H. Weber, Effect of pressure and isotopic substitution on the Raman Spectrumof a-Fe2O3: Identification of two-magnon scattering, Phys. Rev. B41 (1990) 7822-7827
3. O.N. Shebanova, P. Lazor, Raman spectroscopic study of magnetite (FeFe2O4): a new assignment for the vibrational spectrum, Journal of Solid State Chemistry 174 (2003) 424-430
4. M. Chen, J. Shu, X. Xie, H.K. Mao, Natural CaTi2O4-structured FeCr2O4 polymorph in the Suizhou meteorite and its significance in mantle mineralogy, Geochim. Cosmochim. Acta, 67 (2003) 3937-3942
5. B. J. Reddy, R. L. Frost, Spectroscopic characterization of chromite from the Moa-Baracoa Ophiolitic Massif, Cuba, Spectrochim. Acta A 61 (2005) 1721-1728
6. A. Ahlawat, V. G. Sathe, Raman study of NiFe^ nanoparticles, bulk and films: effect of laser power, J. Raman Spectrosc. (2010), (wileyonlinelibrary.com) DOI 10.1002/jrs.2791
206

NOEA2011
Zakopane 4-7 September 2011
PS39
##### Metal-supported sulfated ceria-zirconia catalysts for the SCR of NOX by ethanol: performances and mechanisms A. WESTERMANN1, B. AZAMBRE1*, A. KOCH1
1 Laboratoire de Chimie et Methodologies pour I’Environnement (LCME),
Institut Jean-Barriol, Universite Paul Verlaine - Metz,
Rue Victor Demange 57500 Saint- Avoid, France, *e-mail: bazambre@.univ-metz.fr
In our last study [ 1|, we aimed to investigate the SCR performances and mechanisms of novel sulfated CexZrl.IO2 (SCZ) catalysts using ethanol as reductant. Though these catalysts displayed an intrinsic lesser activity than the widely-studied Ag/Al2O3 and Ag- or Ba-Y catalysts [2], we have shown that the DeNOx yield was strongly dependent on the Ce molar fraction of SCZ catalysts and reached a maximum for x = 0.5 (50 % DeNOx al 350°C) [I], By contrast, the parent sulfated zirconia (SZ) was found to be rather inactive, and sulfated ceria (SC) was less selective than SCZ catalysts, due to its ability to promote the non-selective oxidation of ethanol and the formation of toxic by-products, namely HCN [I], Also, it was noticed that the sulfation treatment of the parent CZ materials partially inhibited the total oxidation of the reductant, rather promoting its partial oxidation to CxHyOz species such as acetaldehyde, which is very selective for the NOx reduction to N2. Hence, sulfated ceria-zirconia have the required characteristics to be employed as supports for EtOH-SCR, and their activity may be possibly further tuned by the help of supported metal promoters, similarly to what we observed previously when these catalysts were investigated for the SCR of NOx by methane [3].
The aim of this article is two-fold: (i) to compare the ethanol-SCR performances of several supported metal catalysts (Pd, Co, Ag on SCZ) with the sulfated support alone; (ii) to assess the influence of the promoter on the different possible reaction pathways for ethanol-SCR.
The parent Cco.2Zr0802 (CZ28) support with tetragonal structure was supplied by Rhodia and had a SBET of 184 m2/g. The sulfated SCZ28 support was obtained by soaking the CZ nanopowder into 0.5 M H2SO4, subsequent drying at 70°C and calcination at 500 °C. Impregnation of SCZ28 with PdCl2, Co(NO3)2 and AgNO3 precursors previously dissolved in NH3, was carried out in order to achieve Pd (0.24 %M), Co (1.03 %M) and Ag (3%w) loadings. Catalytic tests on pre-treated catalysts (500°C under He/O2) were carried out both in ramp (TPSR) and isothermal modes in a quartz reactor in the 25-500 °C range using a standard mixture (unless otherwise staled) of NO (1900 ppm) + EtOH (3020 ppm) + O2 (5 %). The detection/quantification of the reactants/products (more than 10) was done using a FTIR gas cell (2 m) coupled to a Varian Excalibur 4100 FTIR spectrometer and a home-made methodology. N- and C- intermediates adsorbed on the surface were monitored according to the temperature and reaction conditions using a heatable reaction cell coupled to a DRIFTS optical accessory. Bulk and surface characterizations of the catalysts were achieved using TGA, XRD, DRS-UV-Vis, HRTEM-EDX and DRIFTS of CO adsorption al 25 °C.
The nature of promoting species (Pd, Co, Ag) deposited on SCZ28 was investigated first. Prior to SCR catalytic tests, the Pd and Co promoters were found to exist on SCZ surfaces as highly dispersed species, namely |Pd(O)„...H|x+ and [Co(O)n...H]x+, with enhanced Lewis acidity due to the withdrawing effect of sulfate groups. By contrast, a new Ag2SO4 phase was detected by XRD for the Ag catalyst, which coexists with well-dispersed Ag+ and Agnx+ species.
By comparison with the SCZ28 support alone, the NOx conversion on the Co-supported catalyst was somewhat similar (about 40% conversion, namely to N2) but slightly displaced the DeNOx window towards high temperatures (Fig. 1A). By contrast, the presence of Pd and Ag promoters was found to be more detrimental (Fig. I A), as the DeNOx yield decreased by around 12% (42 to 30%). It is worth noting that these results were not that first expected, since the same promoters (especially the Pd one) resulted in a strong enhancement of the DeNOx activity when methane was used instead of ethanol for
207

NOEA2011
Zakopane 4-7 September 2011
NOx-SCR [3]. Hence, this proves that Cex+ species existing on the SCZ28 support are probably the true active sites under the present conditions, i.e. when ethanol is used as reductant.
Figure 1. A) Effect of the promoting species (Pd, Co, Ag) on the NOx conversion under steady-state conditions (NO +C2HSOH +O2); B) In situ DRIFTS spectra of adsorbed intermediates at 350 °C for SCZ28 and Ag/SCZ28
Indirect information about the role of the different promoters and their states under SCR conditions was obtained by comparing: (a) the NOx conversions under TPSR conditions (increasing temperatures, not shown here) with those obtained under steady-state conditions at decreasing temperatures (after TPSR, Fig. 1A)); (b) the temperature-dependence of the main products formed in the gas phase (acetaldehyde, CO, CO2, methane, ethene, ethylnitrite...) or in adsorbed state (ethoxy, acetate/enolate, acetyl, -NC, -NCO, amine-like...). For the promoters investigated, their addition inhibited, at least partially, the Ce active sites and/or the selective oxidation of ethanol to CxHyOz species, which in turn decreases the SCR activity.
More peculiarly, it is worth noting that the DeNOx activity for the Ag-SCZ28 catalyst decreased slightly when switching from TPSR conditions (48% at 415 °C) to isothermal ones (30% at 360 °C). Here, this apparent “deactivation” seems to be related to a decrease in the availability of acetaldehyde (the most selective reductant species) under steady-state conditions, itself due to an in situ reduction of cationic
208

NOEA 2011
Zakopane 4-7 September 2011
Ag species to metallic ones during the test. Such changes in the nature of Ag species were confirmed by XRD and TGA analyses on the spent Ag catalyst, which have pointed out the disappearance of the Ag2SO4 phase under SCR conditions. The decreased NOx conversion in presence of 0.24%WIPd (30% at 350 °C) should also be related to its selectivity for the oxidation of CH3COO' intermediates formed upon CH3CHO adsorption, witnessed by the presence of CO2 and CH4 in rather high amounts.
Finally, this study was completed by the DRIFTS investigation of the SCR mechanism on the support and the Ag-containing catalyst under different conditions. The reactions between nitrates ad-species and some activated forms of HC species (namely from acetaldehyde) was found to be involved directly into the formation of crucial intermediates such as HCN, HNCO, and other ad-species (-CN, -NC, -NCO, NH4+). These intermediates further react with NO and/or O2 to yield N2 via mechanisms rather similar to NH3-SCR.
[1] A. Westermann, B. Azambre, Catal. Today (2010) doi: 10.1016/j.cattod.2010.10.071
[21 Y.H. Yeom, M. Li, W.M.H. Sachtler, E. Weitz, J. Catal. 246 (2007) 413
B. Azambre, L. Zenboury, P. DaCosta, S. Capela, S. Carpentier, A. Westermann, Catal.Today (2011) doi: 10.1016/j.cattod.2010.12.026

INDEX
A
ADAMOWSKAM., 127
ADAMSKI A., 101, 107, 123
ADOUANED.,61, 115
AISSATA.,45, 83, 111
AIBARAZ1 A., 71
ASCASO S„ 77
AZAMBREB.,81, 117, 165,207
B
BANAŚ J., 117
BARTKEJ., 13
BARTOLOMEU R„ 81
BARTOVA Ś., 63, 183
BASSILJ.,71
BERTOLOR.,81
BIAŁAS A., 163
BIELAŃSKA E„ 25, 119
BOICHUK T, 49
BONZI R„ 59
BOUTROS M„ 71
BUZANOWSKI M. A., 23
C
CAMPA M.C., 149
CAMRAJ., 25, 121, 163
CAPELAS., 127
CARRE S„ 67
CASTOLDI L„ 59
CHMIELARZL., 33, 123, 141
CHMIELEWSKI A. G„ 17
CHO B. K„ 55
CHOI J.-S., 63
CHROMCAKOVA Ź., 155
COURCOT D„ 45, 83, 111
CRELLIN C. C„ 55
ĆWIKŁA-BUNDYRAW., 47, 131
D
Da COSTAP., 21,41,61,71,81,89, 115, 127, 165
DARCY P„ 61,89
DHAINAUTE, 67 DJEGA-MARIADASSOU G„ 19,173 DOBIJA A., 135
DOBROSZ-GÓMEZ I., 139,143
DUDEK B„ 123
DUJARDIN C„ 67, 95
DUTKIEWICZ J., 25, 121, 137, 187
DZIEMBAJ R„ 123, 141
DŹWIGAJ S„ 43, 59, 195
E
EMMEZE., 189
F
F1UKM., 107
FOIXM.,21
FONTALVOJ., 143
FORZATTI P„ 59
FOUCHALN., 89
G
GAGNEPA1N L„ 127
GALVEZ M. E„ T1
GHIOTTI G., 59
GIL B„ 27, 29, 107
GOMEZ-GARCIA M. A., 139, 143
GÓRA-MAREK K„ 147
GRADOŃ B„ 99
GRANGER P„ 67,95 GRZYBEK T„ 37
GUYON C.,21
H
HENRIQUES C.,81
HEO I., 55
HILDEN D. L„ 55
HNATI., 195
I
INDOVINA V, 149
J
JANAS J., 43
JAN1GAS., 137, 187
JEANDELX., 115
J1RATOVA K., 97, 155 JODŁOWSKI P„ 27,29
K
KANTCHEVAM., 151
KARASKOVA K., 155
KIM M. K„ 55
KIM P. S„ 55
211

KIRIENKO R, 49, 191
KLINIK J., 37
KNAPIK A., 29
KOCEMBAI., 139, 195
KOCH A., 81, 207
KOĆIK., 159
KOCI P„ 63, 183
KOŁACZKOWSKI S., 27,29, 181
KOŁODZIEJ A., 27, 29
KONKOL M„ 93
KORNELAK P, 137, 163, 165, 167, 187
KOTARBA A., 91, 169, 177
KOVANDA E, 97
KOWALIK P„ 93
KOZICKI M„ 25, 119, 121, 137, 171, 187,205
KREJCIKOVA S„ 159
KRUKJ., 93
KRZTOŃ A., 173, 193
L
ŁABANOWSKA M., 167
ŁACNY Z., 159
ŁAMACZA., 173, 193
LANDI G„ 87
LASEK J„ 99
ŁASOCHA W., 25, 135, 163,175
LAZARO M. J„ 77
LEEJ.-H., 55
LEGUTKO P, 169
LICKIJ., 17
L1ETTI L., 59
LISI L., 87
LITYŃSKA-DOBRZYŃSKAL.,25, 171 ŁOJEWSKA J., 27, 29, 181
M
MACYKW., 167
MAKOWSKI W., 29
MANIAK G„ 91, 177
MANIGRASSOA.,89
MARCEW1CZ-KUBA A., 179
MAREK M., 63, 183 MATUSIEWICZA., 123
Mc CLYMONT D., 27,29, 181 MICHALIK M„ 123 MICHALSKA K., 93 MILANOVAM., 151
MOLENDA M„ 141
MOL1NER R„ 77
MORANDI S., 59
MOTAK M„ 37
MRAĆEK D„ 183
N
NAJBAR M„ 25, 117, 119, 121, 137, 163, 165, 167, 171, 175, 187,205
NAM I.-S., 55
NAZARCZUK I., 25, 119, 137, 167, 175, 187 NAZ1MEK D„ 47
NI X., 95
NITEK W., 135
O
OBALOVA L„ 97, 155, 159
OCHOŃSKA J„ 27, 29, 181
OLSON K., 55
ORLYK S„ 49
ÓZENSOY E„ 69, 189
P
PAŁKOWSKA E„ 25 PALOMARES A. E„ 31 PARTRIDGE W., 63 PAWELEC A., 17 PETELENZ B., 11 PIETRASZEK A., 165 PIETROGIACOMI D„ 149 PIETROWSKI M„ 201
PIHLJ.,63
PIRONE R„ 87
PISKORZ W., 91, 177
PLATE, 183
POPOVYCH N„ 191
R
RADLIK M„ 193
RAFALSKA-ŁASOCHAA., 15, 175 RAS1ŃSKA D„ 163
RENEME Y, 67
RIBEIRO M.E, 81
ROGULSKA A., 29
ROJEK W., 43
RUSSO G„ 87
RUTKOWSKA M„ 123, 141 RYNKOWSKI J„ 195
RYNKOWSKI J. M„ 139, 143
S
SALAUN M„ 127 SAMOJEDEN B„ 37 SEDA §ENTURK G„ 69 SIFFERT S„ 45, 83, III SNAPKAUSKIENE V, 197 SOJKA Z., 91, 101, 107, 169, 177
212

SOLCOVA O., 159
SOLOVIEV S„ 49,191
STAN K., 171
STARCK J., 115
STELMACHOWSKI P.,91, 169,177
STOLECKI K„ 93
STUDENTOVA S„ 155
SU D„ 163
SUNY., 17
SZYNKOWSKAM. I., 139
T
TARACH M„ 107
TATOULIANM.,21
TOBAM., 167
TOBIAS I., 77
TOMSKA-FORALEWSKA I., 201
TORTORELLI M„ 87
TRICHARD J.-M., 53
TUREK W„ 193
V
VAL1NC1US V., 197
VOVK E., 69, 189
W
WĘGRZYNA., 123
WESEŁUCHA-BIRCZYŃSKA A., 25, 163,
205
WESTERMANN A., 81,207
WITMAN S„ 17
WOJCIECHOWSKA M„ 123,201
WU Y„ 95
Z
ZAITZM.M., 141
ZAJĄC W., 101
ZAPAŁA P., 107
ZASADAF.,91, 101, 177
ZENBOURY L„ 165
ZHANG W„ 163
ZHAO Z„ 75
ZIELINSKI M., 201
Z1MEK Z., 17
ZIMOWSKA M„ 119
213