pubs.acs.org/JPCC
Toward the Mechanism of o‑Xylene Isomerization in Selected
Zeolites of Diﬀerent Si/Al Ratios and Channel SizesExperiment Corroborated by Periodic DFT + D Simulations
Gabriela Jajko, Karolina Tarach, Kinga Góra-Marek, Paweł Kozyra, and Witold Piskorz*
Cite This: J. Phys. Chem. C 2021, 125, 10334−10348
Read Online
ACCESS
Metrics & More
Article Recommendations
ABSTRACT: The present work comprises the characterization of zeolite properties in the view of their usability as catalysts in the isomerization of xylenes and ethanol-to-hydrocarbon (ETH) process. Therefore, the intermediate products of these reactions have been proposed as the 5- and 7-membered hydrocarbon ring structures. The quantum chemical calculations were carried out at the periodic DFT GGA + D level of theory to optimize the structures of zeolites and xylenes and the protonated forms of the latter. The isomerization and the ETH processes have similar intermediate products; their identiﬁcation is not, however, possible
spectroscopically; hence, the quantum chemical calculations deemed
necessary. The calculations include thermal eﬀectsthe entropic contributions were calculated via the classic, harmonic vibrational
analysis, and the Gibbs free energies were calculated at T = 298 K, the temperature at which the spectra of gaseous and adsorbed species were recorded. Based on the analysis of the contributions to the adsorption energy of the hydrocarbon 5- and 7-membered ring structures and having veriﬁed the results via comparison of the calculated IR spectra to the experimental ones, the most probable intermediate products were proposed.
■
INTRODUCTION
activity (decreasing with increasing Al concentration). The maximum activity was found for Si/Al ca. 14−15, with a constant p-/o-ratio. The isomerization of xylenes in the wide- pore zeolites (FAU and MOR), with the use of isotopically labeled (deuterated) p-xylene, was also studied experimentally
by Corma et al.,9 who pointed out the discrimination of the mechanism, namely, that on both FAU and MOR, the uni- and bi-molecular isomerization mechanisms can take place, while on BEA, only the unimolecular 1,2-methyl shift can be observed. In the case of ZSM-5, it was found10 that the isomerization of xylenes follows the intramolecular mechanism catalyzed by the Brønsted acid sites (B.a.s.), and the catalytic activity depends on the concentration of reactants on the acid sites which is, in turn, aﬀected by diﬀusion. They also point out that the B.a.s activity depends also on its local environment. The important inﬂuence of diﬀusion on both activity and selectivity for xylene isomerization in ZSM-5 was demon-
Zeolites are crystalline aluminosilicates of high surface area and hydrothermal and thermal stability. Their structural properties responsible for the pores of molecular dimensions and the strong Brønsted and Lewis acid sites provide an advantage in the ﬁeld of heterogeneous catalysis in many major chemical processes.1,2 The expansion of the polymer industry in the last several decades forced the development of eﬀective methods of polymer reactant synthesis. The o-xylene isomerization process was recognized as a feasible method of p-xylene synthesis. Among the three isomers of xylene, p-xylene is the most desirable industrial raw material due to its high demand in the manufacturing of terephthalic acid in the polymer (PET) industry.3 The xylene isomerization reaction can serve also as a model reaction for characterizing the acidity in terms of the number, strength, and location of acid sites and porosity of aluminosilicates as well.
The most successful in xylene isomerization, thus industri- ally common, zeolites are protonic MOR4 and ZSM-55 and, to the less extent, FAU6 and FER.7 The isomerization and disproportionation of m-xylene over the BEA samples with Si/
Al ∈ [11, 42] were studied by Peŕez-Pariente et al.,8 and they
concluded the Si/Al ratio being the decisive factor in the
activity toward the isomerization and disproportionation
© 2021 The Authors. Published by American Chemical Society
https://doi.org/10.1021/acs.jpcc.1c01307
J. Phys. Chem. C 2021, 125, 10334−10348
10334
See https://pubs.acs.org/sharingguidelines for options on how to legitimately share published articles.

Article
Received: February 12, 2021
Revised:	April 20, 2021
Published: May 5, 2021

The Journal of Physical Chemistry C
pubs.acs.org/JPCC
Article
strated much earlier,11−13 where the transition-state selectivity for m-xylene isomerization and its lower diﬀusivity raising the selectivity toward o- and p-xylenes were shown. Very comprehensive studies were provided by Min et al.14 and
others. The overall results of this study provide clear experimental evidence that product shape selectivity is responsible for the high p-xylene selectivity found in some medium-pore zeolites, whereas it is distinguishable from transition structure shape selectivity. The latter is ruled by the bimolecular and unimolecular mechanisms of isomer- ization. The intermediate’s formation energy is only one of the factors inﬂuencing the overall catalytic activity.
In this respect, the recent research work in our group was dedicated to providing an insight into the o-xylene isomer- ization process over the 10-ring zeolites of the diﬀerent pore connectivities and various steric constraints.15−18 Based on the advanced rapid scan FT-IR measurements and the two- dimensional correlation spectroscopy analysis (2D COS) of
the resultant spectroscopic data, it was possible to identify, during the o-xylene isomerization, the intermediate species characterized by the IR bands at 1485 and 1455 cm−1. This method also allowed us to evaluate the mechanism of xylene isomerization over diﬀerent zeolite structures and sequential order of events on the catalyst’s surface. Also, based on the 2D
COS analysis, the mechanism of xylene isomerization over diﬀerent zeolite structures and sequential order of events on the catalyst’s surface were evaluated. The formation of intermediates was found to be dependent on the rigidity of the microporous environment. Moreover, the formation of p- xylene in particular was directly associated with the presence of newly identiﬁed intermediate species and their accumulation in the rigid microporous environment. The structure of the intermediate species remained, however, unknown. The possible transformation of xylenes undergoing protonation includes either the route of insertion of the methylene group into the ring, thus forming the 7-membered ring product, or the paring reaction, where the 5-membered ring intermediate compound is formed.19 Xylenes can be also produced in a feasible non-petroleum route of the alcohol-to-aromatics processes, where methanol or ethanol is converted into aromatics preferably with the high p-xylene content. The conversion of alcohols during the upgrading of natural resources (biomass and natural gas) to aromatics emerges as an interesting alternative of crude oil processing.20,21 The conversion of methanol is investigated comprehensively, but also, ethanol conversion over acidic zeolites is gaining attention
rapidly.22−24
The ethanol conversion to the C3+ hydrocarbons has been
recognized to proceed through a dual-cycle mechanism25 corresponding to the one established for the methanol-to- oleﬁn process.21 This aromatics-based mechanism proposes that the catalytically active sites are the organic−inorganic hybrids of cyclic organic species and zeolite acid sites. The
methylation reaction proceeds with the use of the reactive organic species bound to the zeolite active site, which is
followed by the elimination of products, thus regenerating the initial organic adsorbate.26−29 Further similarities between the methanol and ethanol conversions to higher hydrocarbons are the distributions of formed products.25,30−32 Additionally, the participation of xylenes in the alcohol-to-hydrocarbon process
has been studied by Svelle et al.33 The proposed methylation of toluene by DME led to p-xylene and methanol as one of the possible steps in the hydrocarbon pool mechanism. Since the
methanol and ethanol conversion most probably proceeds through similar paths, understanding the ethanol conversion process can provide signiﬁcant insights into the methanol- based route. The inﬂuence of aromatics on the methanol
conversion reaction was ﬁrst proved by Mole et
al.34,35
The
addition of a small amount of toluene or p-xylene resulted in
an enhanced conversion rate.21 The participation of xylenes in the hydrocarbon pool mechanism prompted our search on similarities in results of the FT-IR spectroscopic observations
cm−1
of both processes. The origin of the 1485
band was
identiﬁed as an intermediate in the xylene isomerization
process since its participation in the ethanol conversion process, presented in this article, was even more stimulating. The necessity of their assessment through the quantum chemical modeling emerges.
In the present article, several intermediate structures (namely, the 5- and 7-membered rings) and parent o-xylene, together with their IR spectra, were proposed and veriﬁed. As the FT-IR spectroscopy supported by 2D COS allowed us to gain signiﬁcant insights into the xylene transformation process, the same methodology was applied to follow the changes in FT-IR spectra during the ethanol conversion process. The 2D COS analysis, developed by Noda,36 is herein coupled with standard and rapid scan time-resolved in situ FT-IR spectros- copy. The tracking of the slightest changes in the FT-IR spectra of the catalyst surface during the reaction and the
detection of intermediate products are possible.
■
EXPERIMENTAL SECTION
Materials. The NH4ZSM-5 zeolite with a Si/Al ratio of 12
was purchased from Zeolyst Int. (CBV 2314). The protonic form of ZSM-5 zeolite was obtained by calcination under static air at 580 °C for 3 h with a heating rate of 1 °C/min; the β
parent zeolite (NH4β) was purchased from Zeolyst (CP814C). The native MOR zeolite was bought also from Zeolyst International, (CBV 10A). Chabazite was bought from Clariant. The TNU-9 zeolite was synthesized using 1,4- bis(N-methylpyrrolidinium)butane dibromide (1,4-MPB) as a template formed in situ by reaction between 1,4-dibromobu- tane (1,4-DBB) and 1-methylpyrrolidine (1-MP). In a typical synthesis, the ﬁnal gel contained 4.5 (1,4-DBB)/13.5 (1-MP)/ 11 (Na2O)/0.5 (Al2O3)/30 (SiO2)/1200 (H2O). The gel was
stirred at room temperature for 1 h and then transferred to Teﬂon-lined 35 mL autoclaves. The synthesis proceeded at 160 °C for 8 days under agitation and autogenic pressure. The solid products were recovered by ﬁltration, repeatedly washed with water, and then dried overnight at 100 °C. All hydrocarbons (from Sigma-Aldrich) used in this study were of 99% purity.
FT-IR Spectroscopy Studies. The self-supporting discs of studied samples were prepared (ca. 5 mg/cm2) and evacuated in a quartz cell with CaF2 windows at 530 °C under vacuum for 60 min. The adsorption of carbon monoxide (CO) was performed at −100 °C and that of ammonia (NH3) was
performed at 170 °C.37,38
Acid strength of sites was determined in CO adsorption and NH3 thermodesorption experiments. The formation of a hydrogen bond between CO and the bridging hydroxyls of the original Si(OH)Al band in zeolites is responsible for the down shift of the band (ΔμOH···CO). The higher the strength of
the acidic proton in the Si(OH)Al unit, the higher the down shift is observed. The acid strength detection in NH3 thermodesorption is performed as follows. In the ﬁrst stage
https://doi.org/10.1021/acs.jpcc.1c01307
J. Phys. Chem. C 2021, 125, 10334−10348
10335

The Journal of Physical Chemistry C
pubs.acs.org/JPCC
Article
of the experiment, all acid sites were neutralized with ammonia, while physisorbed molecules were removed by evacuation at 170 °C. In the second step, desorption was carried out at the two following temperatures: 330 and 450 °C. The ratios A330/A170 and A450/A170, where A170, A330, and A450
The stable geometries for each postulated reaction elementary step were determined with the use of the BFGS algorithm.47,48 The (vibrational) entropic contributions were calculated via the classic, harmonic vibrational analysis, and the Gibbs free energies were calculated at T = 298 K, at the same temperature at which the spectra of gaseous and adsorbed species were recorded. The transition states were located starting with the LST/QST guess,49 followed by the BFGS50 reﬁnement, and then veriﬁed by the vibrational analysis, under the condition of only one negative Hessian eigenvalue appearing among the calculated normal vibrations. The atomic charges and bond orders were obtained within the Hirshfeld51 and Mayer52 analyses, respectively.
Models. Distribution of Al Sites. Based on the
experimental value of Si/Al, the number of aluminum atoms per unit cell was determined as follows: 6 out of 96 in MFI, 4 out of 64 in BEA, 3 out of 12 in CHA, 5 out of 48 in MOR, and 14 out of 192 in TNU-9 (Table 1). It is generally assumed
are the intensities of the NH + band (1450 cm−1) measured
4
after each desorption step, were taken as the measure of the acid strength of protonic sites.
Sorption of o-xylene (analytical grade, 99% purity) on the zeolite samples (ca. 45 mg) was performed at 250 °C. The materials were contacted with o-xylene vapor (4 Torr = 0.53 kPa); the reaction was proceeded for 15 min, and then, the temperature was lowered to RT, and spectra were collected. Sorption of ethanol (40 Torr = 5.3 kPa) on the zeolites was also carried out at 250 °C. The spectra were collected for 120 min every 8 s. The analysis of spectra has been divided into two separate stages of reaction before and after 10 min from the reaction beginning. Two-dimensional correlation spectros- copy was performed over recorded 1D spectra in these two
time domains.
All the spectra were recorded with a Bruker Vertex 70 spectrometer equipped with an MCT detector. The spectral resolution was 2 cm−1. The 2D COS graphs were prepared with the use of OPUS 3D software from Bruker Optics and OriginPro 9.1.
Computational Details. All the quantum chemical
calculations of energies, geometries and vibrational analyses were performed with the use of the DMol339 code at the periodic DFT level of theory, with the RPBE40,41 correlation- exchange functional. This functional was chosen based on the conclusion that it is a good compromise in many cases when gas-phase molecules and solids are treated simultaneously, particularly because it provides a better description of the hydrogen bonds than PBE or revPBE. The orbitals were expanded in the basis set of DND quality with the DSPP pseudopotentials.42 A basis set spatial cutoﬀ distance of 4.5 Å was set and, as a convergence accelerator, the Gaussian
smearing with a window width of 5 × 10−3 Ha was used. The SCF convergence criterion was set to 1 × 10−6 Ha, whereas for geometry optimization the convergence criteria were as
follows: for the energy change between two successive iterations the value of 2 × 10−5 Ha was used, for the gradient norm the threshold of 4 × 10−3 Ha/Å was applied, and for the maximal atom displacement the value of 5 × 10−3 Å was used.
Due to the large unit cell size of ZSM-5, MOR, and TNU-9, the Γ-point-only sampling of the IBZ (irreducible part of the ﬁrst Brillouin zone) was found to be suﬃcient. For smaller unit
cells (CHA), however, the IBZ was sampled due to the Monkhorst−Pack algorithm with a k-point density of 3 × 3 ×
3. In all cases, the k-point separation in the reciprocal cell was
suﬃcient, taking into account the calculations of the time- consuming vibrational analysis, ca. (0.05 × 0.05 × 0.07) Å−3, (0.06 × 0.05 × 0.13) Å−3, and (0.10 × 0.10 × 0.10) Å−3, in the
case of ZSM-5, MOR, and CHA zeolites, respectively (denser than the rule-of-thumb recommended value: 0.05 × 2π/Å for insulators). The London dispersion eﬀects, important for the description of the zeolite−hydrocarbon interactions,43,44 were accounted for by the semi-empirical correction to the DFT functional in a post-SCF manner, using the pairwise interatomic interactions dependent also on the charge density.45 The unit cell parameters were optimized by ﬁtting the energy−volume relationship to the Birch−Murnaghan equation of state.46
Table 1. Si/Al Values and the Channel Member Ring Count of the Studied Zeolites
MR
Si/Al
12
15
8
3
10
15
12/8
8.6
10
14
that the
aluminum
atoms
in zeolites
are not
distributed
randomly but also not periodically; thus, their localization is not unambiguously assessed and is diﬃcult to determine. Some
information on aluminum distribution is, however, available for
BEA,53 MFI,54,55 CHA,56 MOR,57 and TNU-9;58 namely, for
BEA, the preferable localization of Al is T5, for CHAT1, for
MFIT10, T7, and T12, for MORT3, and for TNU-9 T2, T8, T11, T14, and T21, and these positions were exchanged by Al in this work. The location of aluminum and OH groups may be found in Figure 1. In our models, Al atoms are isolated except for BEA, so they should be referred to experiments for either zeolite of small amounts of Al pairs (ZSM-5(S)) or for high-acidic OH groups.59 The OH groups have been located at the positions adjacent to the Al atoms. The OH group interacting with the o-xylene molecule has been chosen based on the accessibility, so that it points into the largest void possible, namely, into the channel (or the widest
channel, if the channels of various sizes exist).
■
RESULTS AND DISCUSSION
FT-IR Studies of Ethanol Transformation over ZSM-5
Zeolite. The FT-IR spectra of ethanol transformation at 250
°C in ZSM-5 are presented in Figure 2. At the ﬁrst stage of the
reaction process, the formation of ethylene (2990 and 1888 cm−1) is observed, which is next transformed into the higher hydrocarbons. The water molecules generated at elevated
temperature of performed reaction are not able to adsorb on the Si(OH)Al, and water is detected only in the gas phase.
The complex nature of the undergoing ethanol-to-hydro- carbon (ETHs) process was investigated with 2D COS analysis. The overlapping of the diagnostic bands and the formation of various intermediates and products of reaction make the analysis of spectra challenging. The 2D COS analysis of collected spectra in the asynchronous mode allowed us to establish also the sequential order of events taking place on the catalyst surface. The 2D contour maps with the levels of changes in spectra are presented with two axes for wave-

https://doi.org/10.1021/acs.jpcc.1c01307
J. Phys. Chem. C 2021, 125, 10334−10348
10336
zeolite	BEA	CHA	MFI	MOR	TNU-9

The Journal of Physical Chemistry C
pubs.acs.org/JPCC
Article
Figure 1. Optimized o-xylene molecule positions together with the location of the OH group (red clouds) in the channels of BEA, CHA, MFI, and MOR (ﬁrst two rows) together with the optimized position of DFM in the channel of TNU-9. The linear scale of distances is preserved among structures.
and 1495 and 1474 and 1375 cm−1 bands (Figure 3A). The asynchronous maps provide information on the sequential order of events occurring on the zeolite surface during the
reaction. Based on the analysis of the asynchronous map (Figure 3B), it can be inferred that the increase in the 1375
numbers and one for the correlation level. The 2D maps possess much sharper and easier resolved peaks than the parent 1D spectra and can provide valuable insights into the following surface reactions.
The scrutiny of undergoing reaction was performed for two separate time domains: before (Figure 3) and after 10 min (Figure 4) from the introduction of ethanol. Synchronous maps of 2D COS analysis provided information on the direction of changes in the bands’ intensities. First, the negative
cm−1
cm−1
band was followed by the increase in the 1507
band, and then, the 1485 cm−1 band decrease occurred. The
next stage of the reaction process was described only by positive correlations on the synchronous map (Figure 4A), that
is, 1600 and 1507 cm−1 and 1495 and 1474 and 1386 and 1375 cm−1 bands. The asynchronous map (Figure 4B) proved that the sequential order of band intensity changes is as follows:
cm−1
correlations of the 1507 and 1485
bands and between
1485 and the set of bands, denoted hereafter with ampersand,
cm−1
1588 and 1375
were found. The band transformation,
cm−1
cm−1
one into another, represented by abovementioned negative correlations, is accompanied also by the positive correlation, that is, the simultaneous changes in band intensities in the
1600 and 1495
bands increase before the 1508
band. The presence of the aromatic species, for example,
cm−1
polymethylated benzenes (the 1507
band is typical of
same direction. The positive correlations during the ﬁrst 10 min of the reaction are found between 1507 cm−1 and 1588
1,2,4-trimethylbenzene) on the zeolite surface conﬁrms that
the aromatics-based hydrocarbon pool mechanism is occurring

https://doi.org/10.1021/acs.jpcc.1c01307
J. Phys. Chem. C 2021, 125, 10334−10348
10337

The Journal of Physical Chemistry C
pubs.acs.org/JPCC
Article
Figure 2. Red lines: FT-IR spectra of ethanol adsorbed in ZSM-5 successively collected at 250 °C every 5 min of reaction; dark gray line: spectrum of activated ZSM-5 before the sorption of ethanol.
Figure 3. 2D correlation maps (Asynchronous, Basynchronous) in the CHx bending vibration region for the ETH reaction for the ﬁrst 600 s of the process at 250 °C.
Figure 4. 2D correlation maps (Asynchronous, Basynchronous) in the CHx bending vibration region for the ETH reaction after 600 s of the process at 250 °C.
under our applied experimental conditions. Besides 1,2,4- TMB, also, benzene (1474 cm−1 diagnostic band) and toluene
intermediate species found during the xylene isomerization process has been identiﬁed also during the ETH process, and the 2D COS analysis conﬁrmed its transformation into the
cm−1
diagnostic band) can be identiﬁed during the
(1495
cm−1
cm−1
reaction process. Most importantly, the 1485
band of
1507
band representative for 1,2,4-TMB. Previously, it

https://doi.org/10.1021/acs.jpcc.1c01307
J. Phys. Chem. C 2021, 125, 10334−10348
10338

The Journal of Physical Chemistry C
pubs.acs.org/JPCC
Article
be induced by the diﬀusion constraints in 10-ring channels. The ZSM-5 zeolite among diﬀerent zeolite structures was studied most extensively as highly suitable for xylene isomerization.
Diagnostic Band. The experimental FT-IR spectra and the
vibrational analysis for the considered intermediates brought independent and compatible information, for example, the presence of the diagnostic band at ca. 1485 cm−1 (Figure 5).
was shown that in the TNU-9 zeolite, even in the lower temperature region, the formation of polymethylated benzenes occurred;17 the ZSM-5 zeolite requires, however, higher temperatures for 1,2,4-TMB observation during ethanol transformation. The discrimination between the 1,2,4- trimethylbenzene and 1,2,4-triethylbenzene under our exper- imental conditions is highly diﬃcult, as IR spectra of both show high similarities; thus, it must be taken into account that even if the products of the ETH and mETH process are identical, the intermediates may diﬀer with some preferences to polyethylated benzenes when ethanol is considered. The accumulation of reaction products in the second part of the process and lack of negative correlations suggest that the hydrocarbon pool initiation was ﬁnalized, and steady-state reaction products, partially accumulated on the surface, are in majority realized to the gas phase. The formation and accumulation of the aromatic species are observed as abovementioned positive correlation between the set of
bands (1600 & 1507 and 1495 & 1474 cm−1); this is also accompanied by a relatively high correlation level from C−H bending vibrations bands (1386 and 1375 cm−1) (Table 2).
Figure 5. Intermediate’s IR band upon o-xylene adsorption on CHA, MFI, MOR, and BEA.
Table 2. IR Band Assignment
cm−1
Additionally, it was proved that the band at 2740
is
associated with the presence of the intermediate diagnostic
band.16 On the other hand, for both gas-phase and physisorbed
2990, 1888
2740
ethylene in the gas phase
intermediate: methylbenzenium ion (aromaticC−H stretching)
condensed aromatic species
1,2,4-trimethylbenzene (C−C stretches in the aromatic ring)
toluene (C−C stretches in the aromatic ring) intermediate: xylenium ion
benzene (ν19 C−C vibration of the aromatic ring) intermediate: diphenyl methane (scissoring vibration of
CH2)
C−Hx bending modes
cm−1
o-xylene, the 1485
band is not observed. The
experimental Fourier transform infrared (FT-IR) spectra
presented in this paper for several additional zeolite structures, CHA, MFI, MOR, and BEA, after the in situ isomerization of
1600, 1588
1507
cm−1
o-xylene (Figure 5) prove that the 1485
band can be
detected also in other zeolite structures. The smaller the cavity formed by intersecting channels (BEA, MOR, and MFI) or
1495
1485
1474
1455
cm−1
cages (CHA), the higher intensity of the 1485
band
detected in the IR spectra. The vibrational analysis for the gas-
phase o-xylene molecule reveals the strong bands at ca. 1473
and 2939 cm−1none were found close to 1485 cm−1. In the case of the physisorbed o-xylene, the strong bands occur at
1386, 1375
cm−1
cm−1
FT-IR Studies of o-Xylene Transformation. Previously, it was proved that the microporous structures such as ZSM-5, IM-5, and TNU-9 deliver diﬀerentiated catalytic performance in methanol-to-hydrocarbon,21,60 ETH,17 and xylene isomer- ization processes.15 The 2D COS analysis showed that the o- xylene transformation is strongly inﬂuenced by the diﬀusion of the reagents in a microporous environment. The formation of intermediate species characterized by IR bands at 1485 and
1455 cm−1 was recognized. The latter can be assigned to the
scissoring vibration of CH2 in diphenyl methane. Their
amount was associated to the rigidity of the microporous system: the most spacious environment for o-xylene trans- formation was characterized by the lowest population of intermediates, whereas structures oﬀering a suﬃciently tight geometry accommodated intermediate species in higher quantities, ﬁnally leading to the production of p-xylene with high selectivity.15 The analysis of the inﬂuence of the acid site location and its strength on the xylene isomerization process was also followed using the FT-IR spectroscopy and 2D COS analysis.18 Among ZSM-5 zeolites of diﬀerent Si/Al ratios, the isomerization reaction proceeded eﬀectively over ZSM-5 zeolites of Si/Al between 10 and 30. The reduction of Brønsted acid site density, that is, the increase in Si/Al, enabled the disproportionation path (zeolites of Si/Al higher than 40). The formation of intermediate species was found to
1389 and 2975
for MFI, at 1392 and 2955
for
MOR, at 1224 and 3052 cm−1 for CHA, and at 1411 and 2770 cm−1 for BEA.
cm−1
In Table 3, the calculated bands at ca. 1485
are
gathered for all structures of zeolites and all considered
intermediates which yield the diagnostic band. Only for the
cm−1
C5o structure, the band at ca. 1485
appears for all
studied zeolites, making this structure the most probable as an
intermediate. Surprisingly, all structures have positive for- mation energy in mordenite, and still, C5o has the lowest energy. Taking into account, however, that bulkier (C7) intermediates cannot be formed in 8-membered channels (CHA), the C7-4 structure is possible for MFI, MOR, and BEA.
We have found that the 1485 cm−1 band corresponds to the
cm−1
deformation vibrations (e.g., 1486 and 1487
bands in
MFI are the CH2 scissoring vibration of the CH3 group). For CHA, the 1486 cm−1 band is the scissoring and twisting of the
CH3 group with the admixture of the ring deformation. Hence, the presence of the 1485 cm−1 band can be regarded as the
indicator of the o-xylene protonation.
Structure of Intermediates. The total number of 18 hydrocarbon C5 and C7 candidates for being the intermediates in the intramolecular mechanism has been considered; their structures are presented in Figure 6.
https://doi.org/10.1021/acs.jpcc.1c01307
J. Phys. Chem. C 2021, 125, 10334−10348
10339
band position in
cm−1	assignment

The Journal of Physical Chemistry C
pubs.acs.org/JPCC
zeolite deprotonation energy (ΔGdp), and the interaction energy (ΔGint)
Table 3. Resultant (DFT Calculated) IR Bands (Diagnostic,
at ca. 1485 cm−1, in the Range ±10 cm−1, in Parenthesis
Bands of Very Low Intensity, ItalicPositive Low
Formation Energy, BoldNegative Formation Energy) for Postulated Intermediates in Studied Zeolites
ΔG (Z , I) = ΔG (I) + ΔG (Z) + ΔG (Z , I)
(1)
f
pr
dp
int
The contributions to adsorption energy are, to some extent, mutually independent as the protonation energy depends on the kind of intermediate “(I)” only and the deprotonation energy depends on zeolite “(Z)” only, while the energy of the interaction between zeolite and the protonated form of xylene depends on both zeolite and the intermediate structure “(Z, I)”. Stabilization of a given intermediate is determined by the interplay between the stabilization eﬀects: ΔGint < 0 and ΔGpr
< 0 and endothermic eﬀect ΔGdp > 0. The energy necessary to break the O−H bond is so high that proton transfer energy, ΔGtr = ΔGpr + ΔGdp, is always positive.
For the total adsorption energy to be negative or at least as low as possible, the energy of deprotonation should be relatively low, while, at the same time, the protonation energy
+
C5o C5m C7-1 C7-2 C7-3 C7-4 C7-5 C7-9 C7-9t C7-10 C7-11 C7-12 C7-13
1487
1483
1478
1485
1482
1480
(1481)
1477
1482
1483
1480
1479
1486
1488
1476
1484
1480
1486
1477
1486
1478
1488
1481
(1487)
1487
1491
and the energy of C8H	cation interaction with the
1486
(1492)
11
deprotonated zeolite should be relatively high to the absolute value (high stabilization). As will be discussed later, such a coincidence among approximately 75 considered systems is quite rare.
Protonation Energy. The stability of isolated considered
Adsorption Energy. Adsorption of o-xylene leads to the protonated forms before it is transformed into other isomers.
The energetic eﬀect of forming such protonated xylenes
intermediates (Figure 6) varies in quite a wide range (ΔGpr,
(denoted hereafter as ΔEfelectronic energy; ΔGffree
see Figure 7)its variability between structures reaches about 50 kcal/mol (up to about 100 kcal/mol); thus, it gives the large contribution to the diﬀerentiation of the overall
energy at 298 K) can be decomposed into three
componentsthe xylene protonation energy (ΔGpr), the
Figure 6. Sketch of the C7 and C5 intermediates considered in this article.
10340
https://doi.org/10.1021/acs.jpcc.1c01307
J. Phys. Chem. C 2021, 125, 10334−10348
Article

MFI	MOR	CHA
intermediate	wavenumber/cm−1
BEA

The Journal of Physical Chemistry C
pubs.acs.org/JPCC
Article
cannot be directly estimated from the A330/A170 values, as an
additional eﬀect (conﬁnement eﬀect) contributes to the NH +
4
A330/A170
ion stabilization. The
measure is indeed a super-
position of three eﬀects, as was said before: the deprotonation energy and the conﬁnement eﬀect.
ΔνÕH···CO,
The latter quantity,
is the downshift of the
wavenumber of the OH stretching band upon adsorption of
CO. However, the measured and calculated enthalpy points toward MFI as the least acidic. The obtained results are in line with those obtained by Boronat and Corma,61 who also note that the discrepancies between diﬀerent acidity measures do not prejudge their usability since those measures are prone to other factors such as the channel size or structure, which contribute to the overall eﬀect of conﬁnement.
The conﬁnement eﬀect, introduced by Derouane et al.,62
assumes the inﬂuence of the curvature of the zeolite pores and cages on the reactivity via the long-range dispersion interaction. This eﬀect is contrary to the shape selectivity (with respect to the reactants, products, or transition structures), which rather stems from the short-range Pauli repulsion.63 It can rationalize the observation that mordenite and chabazite, having 8-membered ring channels, show overestimated values of adsorption energy, both computed and registered experimentally, compared to MFI and BEA, despite the former’s lower acid strength.
The recent computational work of Iglesia reviews a plethora of articles and discusses the reactivity descriptors as being determined by the properties of both acid sites and adsorbed molecules. The properties actually concern the proton donor and acceptor properties. This is criticized by the authors, and the necessity of inclusion of energy- minimizing charge reorganization is emphasized. The importance of the conﬁnement eﬀect, as the tendency of the guest and host to undergo the electrostatically driven mutual geometrical ﬁt, even at the expense of the reorganization energy, is also accented.
In this spirit, the more detailed decomposition of the acid site−molecule interaction is performed.
As was pointed out by Boronat and Corma,61 some bases can be used to “measure” the acid strength of the centers if the
diﬀerent proton aﬃnity is taken into account. Indeed, for a selected set of intermediates, here, six out of 18 (see Figure 8) heat formations depend mainly on proton aﬃnity due to the similar conﬁnement eﬀect. It cannot be, however, regarded as a general rule for intermediates (even those of similar size). Taking into account that ΔGdp is almost constant, the deviation of heat formation is essentially due to ΔGint values (see Figure 9). The described dependencies indicate that the acidity of centers which protonate xylene molecules rises in the
sequence of MFI ≈ CHA < BEA (in Figure 9 the acidity rises from the left top corner toward the right bottom corner).
Figure 7. Calculated protonation energy, ΔGpr, of o-xylene toward formation of diﬀerent intermediates.
formation energy (ΔGf). Based on the protonation energy, the candidates for intermediates can be indicated. Among the structures containing a pseudo-5-membered ring, the C5o structure is the most stable, while C7-2 and C7-3 are the most stable among the 7-membered ring structures. On the other hand, the C7-9 structure is deﬁnitely the least stable because one of the carbon atoms contains a lone electron pair.
Deprotonation Energy. As it was mentioned before, ΔGpr does not depend on the zeolite structure, while the deprotonation energy, ΔGdp, depends on zeolite only. The data concerning zeolite ΔGdp parameters gathered in Table 4 are ambiguous. On one hand, there is a variety of measures of acidity, and on the other hand, the OH groups are heterogeneous due to the location and Al distribution. All experimental measures (Table 4) present the same trend: for zeolites without 8-membered ring channels, the acid strength relationship is MFI > BEA; for zeolites with 8-membered ring channels, the acid strength for CHA is higher than for MOR. The deprotonation energy, ΔGdp, does not exhibit a very large diversity for the considered structures (ca. 6 kcal/mol).
Acid Strength Measures. The strength of acid sites can
be assessed with the use of a few measures; often, they are the
64
experimental ammonia desorption ratio,
A330/A170
(ratio of
absorbance measured at 330 °C versus absorbance at 170 °C),
and the OH band red shift upon CO adsorption (ΔνÕH···CO).
The former measure,
A330/A170,
should be, however,
considered with due bias. Namely, the ammonium cation
interacts very strongly with the zeolite framework oxygen, and the interaction is particularly pronounced in the structures
consisting of 8-ring channels, for example, MOR and CHA
(conﬁnement eﬀect, vide infra)this is in line with our
ﬁndings. Consequently, information on proton acid strength
Table 4. DFT + D Deprotonation Energies (Gibbs Free Energy ΔGdp at T = 298 K, Adiabatic Energy ΔEv+r, Vertical Energy
dp
ΔEver, Relaxation Energy ΔErel), and the Vertical Electron Detachment Energy ΔE	(Negative Electron Aﬃnity), Calculated
dp
a dp
ved
for Studied Zeolite Models
−31
−28
−24
−31
168
162
164
172
MFI MOR CHA BEA
248
249
243
247
251
255
250
253
282
283
274
284
3587
3560
3595
3521
0.987
0.988
0.987
0.991
138.0
136.0
134.0
132.7
4.45
7.15
6.35
4.93
aThe letter α denotes the ∠(Al−O(H)−Si) angle. All energies are in kcal/mol.
10341
https://doi.org/10.1021/acs.jpcc.1c01307
J. Phys. Chem. C 2021, 125, 10334−10348
ΔGdp	ΔEv+r	ΔEver	ΔErel	ΔE	ν/̃cm−1	rOH/Å	α/deg	r	/Å
dp	dp	dp	ved	Al−Al

The Journal of Physical Chemistry C
pubs.acs.org/JPCC
Article
the highest for this zeolite, indicating the overwhelming impact of the conﬁnement eﬀect on the ammonia stabilization. The
relaxation energy (ΔErel) compensates signiﬁcantly the
variation in ΔE the higher ΔE , the higher value of Δ
dp
ver
ver
rel
E ,
dp
dp
dp
and ΔG	are very similar for diﬀerent
ΔEv+r
and hence
dp
dp
zeolites. Experimental acid strength measure (ammonia desorption ratio, A330/A170) and the OH band red shift upon
(ΔνÕH···CO)18
correlate well with the ∠(Al−
CO adsorption
O(H)−Si) angle (Table 5).
The following factors could be identiﬁed as inﬂuencing the
Brønsted acid strength: (i) the local structure of the center and
(ii) the interaction with the channel wall, namely, with wall oxygen atoms located above the adsorbed molecule (in the
framework orientation when the OH group is located at the
bottom of the channel)the eﬀect “from the top”.70 Some properties, for example, ∠(Al−O(H)−Si), are relevant for the local properties, while the other are for the overall eﬀect. The “from the top” interaction modulates ν,̃which increases due to the increased polarization of the OH group.70 It is also aﬀected
by the distance between the Al−OH group and the closest Al atom (rAl−Al); thus, in the case of MFI, ν̃for the OH group adjacent to the Al site is blue-shifted because of its proximity to
the next Al, what stems from the high “local concentration” of Al sites (low Si/Al ratio). In the case of BEA, however, contrary to the eﬀect of the small ∠(Al−O(H)−Si) angle, the
Figure 8. Correlation between the formation energy and protonation energy of o-xylene transformation intermediates. The C7 structures, in the order from the lowest to highest proton aﬃnity: C7-9, C7-5, C7- 10, C7-8, C7-4, and C7-7, are presented. Inspired by ref 61.
Similar conclusions can be inferred from the magnitude of ν̃
(lowest for BEA) and	(highest for BEA), see Table 4, which indicates their adequacy as the measure of acid strength.
rOH
low ΔHads(NH3) energy, and the short
rAl−Al
distance, this
zeolite has unexpectedly low ν̃and long rOH distance, what can
The deprotonation energy (ΔEv+r) can be decomposed into
be rationalized by the “from the top” eﬀect, namely, the interaction with zeolite framework walls.
The energy of the vertical electron detachment from the acid
dp
two contributions: the vertical proton detachment (ΔEdp ,
ver
proton detachment without relaxation of the rest of the
system) and the relaxation energy (ΔErel, geometry change
ΔEved
(negative electron aﬃnity), discussed in the
dp
residue,
energy imposed by deprotonation). The values of the Gibbs free energy (vibrational entropy), the adiabatic energy, the vertical energy, and the relaxation energy are also gathered in Table 4.
literature as the measure of the acid strength of strong acids
and superacids,71,72 does not discriminate, however, studied zeolites relevantly. The protonation of xylenes requires the acidic property of the zeolite, and all of the considered zeolites are acidic enough to protonate o-xylene, and the other factors determine the prevailing path of the reaction. The OH group strength cannot be, therefore, regarded as the determining factor in the isomerization process in studied zeolites.
Interaction Energy. The last component of the formation
of the intermediate, according to eq 1, is the energy of the
ΔEver can be considered as a measure of the energy barrier in
dp
the detachment of the proton process (despite the fact that
after detachment of H+, the structure relaxes) and, in that way, a measure of acid strength. To the best of our knowledge,
neither ΔEver nor ΔErel has been used for the estimation of acid
dp
dp
strength in zeolites before. It seems, however, justiﬁed as the
quantity ΔEver was successfully used for the calculation of the
dp
65
interaction of the C H + cation with the anion of the zeolite
acidic dissociation constants in solutions. The vertical energy of deprotonation changes in a broader range than ΔGdp and is the lowest for CHA, while the ammonia adsorption energy is
8 11
framework, ΔEint(Z, I), which depends on the structure of
both the cation and zeolite (Figure 9).
Figure 9. Interaction energy of possible intermediates and the zeolite anion.
10342
https://doi.org/10.1021/acs.jpcc.1c01307
J. Phys. Chem. C 2021, 125, 10334−10348

The Journal of Physical Chemistry C
pubs.acs.org/JPCC
Article
Table 5. Experimental NH3 Adsorption Enthalpy, ΔHads(NH3), NH3 Desorption Ratio, A330/A170 and A450/A170, and the OH Band Red Shift Upon CO Adsorption, ΔνOH···CO
−34.766
−34.667
−38.366
−41.868
−32.369
−30.869
MFI
0.91
0.20
315
3603
MOR
0.6 +
0.35
309
3600
CHA BEA
0.78
0.5
0.45
0.15
3610, 3565
3609
309
Figure 10. Formation energy, ΔEf, (deﬁned according to eq 1), of possible C5 and C7 intermediates in studied zeolites (silicalite forms). The negative value means a stable structure.

Adsorption EnergySummary. As it was mentioned
before, the factors other than the strength of Si(OH)Al sites determine the prevailing path of the reaction. It can be seen that the cation structure has a greater impact on ΔEint(Z, I). This variation, however, is compensated to a large extent by
the protonation energy. This becomes noticeable after adding
up all the contributions (Figure 10)the diﬀerentiation of the overall energy, among 18 intermediates, is lower than when considering particulate energy components. In this case, the total energy for the C7-9 structure is also the most unfavorable. In most cases, the intermediate formation energy, ΔEf, reaches
about 5−20 kcal/mol. For some combinations of the
intermediate andzeolite, however, the value of the formation
energy is close to zero, including C7-1, C7-2, C7-3, C7-6, C7- 7, and C5m in MFI and C7-7, C7-9t, C7-12, and C5m in CHA, and for several cases, it reaches negative values: C5o in MFI, BEA, and CHA and C7-12 in MFI. Still, the intermediate
products are only weakly stabilized in the wide-pore structures (MOR and BEA), and consequently, the 1485 cm−1 bands are weak or even absent (Figure 5). The C5o intermediate is most stable in MFI and CHA; however, for the latter, the diﬀusion limitation is critical. In the 12-MR zeolites, additionally,
another intermediate can be postulated, namely, C7-12 (see Figure 11).
The formation energies, averaged over all structures, indicate that they are similar to each other for MFI and CHA (they are also the lowest), higher for MOR, and the highest for BEA
Figure 11. Formation energy of the most stable C5o and C7-12 intermediates in the studied zeolites.
zeolite: 10.7, 12.3, 17.6, and 22.3 kcal/mol, respectively. It is
correlated with the size of the poresBEA zeolite has 12- membered ring channels, and MOR has both 12- and 8- membered ring channels, while the access of xylenes to the MFI channels and the CHA cages is ruled by the 10- and 8- membered rings, respectively. Based on this analysis, it can be

https://doi.org/10.1021/acs.jpcc.1c01307
J. Phys. Chem. C 2021, 125, 10334−10348
10343
ΔHads(NH3)	A330/A170	A450/A170	ΔνÕH···CO/cm−1	νÕH/cm−1

The Journal of Physical Chemistry C
pubs.acs.org/JPCC
Article
can also have a diﬀerent origin. On the other hand, the CH2 band could be too weak to be visible in the spectrum despite the presence of DFM in the sample (e.g., MFI). The experimental solution for the issue of the DFM formation in the studied system could be the adsorption of DFM at the temperature at which it does not react. Based on the DFT
calculations, it can be predicted that the band at ca. 1455 cm−1
can be observed for DFM formed in MOR and BEA (boldface
values in Table 6). In the case of TNU, the vibrational analysis was performed with partial Hessian (limited to the DFM molecule). Computed wavenumbers indicate scissoring
vibration and are close to 1455 cm−1. According to the
calculations, for the DFM molecule adsorbed in TNU, at least
concluded that the intermediate products are better stabilized in zeolites with a smaller pore structure. These results are also in line with IR experiment, namely, the band at 1485 cm−1, attributed to the intermediate (Figure 5), has a high intensity for small pore zeolites such as CHA or MFI and low for large
pore structures, MOR and BEA. CHA was chosen for modeling to show that o-xylene cannot ﬁt into the channels, so, moreover, it cannot diﬀuse through the 6-MR windows in the structure. It is, however, possible to compare the experimental results to the computational results due to the interaction of the o-xylene molecules with the channel openings at the external surface of the zeolite grains. Still, such adsorbed structures yield the bands of only very weak intensities; thus, the relative intensities of the band at 1485
cm−1
two vibrations with wavenumbers close to 1455
are
cm−1
were used in Figure 5 (the spectrum of CHA was
observed (Table 6). The band intensities, however, have not been calculated, so more precaution should be taken due to the
multiplied by 10). Nonetheless, for the high-quality spectra, it
is possible to register such bands above the noise level. Indeed, comparing the stabilization energies of o-, m-, and p-xylene in CHA, it can be seen that the former two isomers are much less stabilized, and they are also less stable compared to those in MOR and MFI (see Table 7).
Intermolecular Mechanism. In possible xylene isomer-
ization pathways, the intra- or intermolecular mechanisms are usually taken into account. In the latter case, the diphenyl- methane (DFM) molecule is considered the intermediate.14 In the 10-ring or wider channels, the intermolecular mechanism is
less-reliable computational methodology used, especially taking into account that TNU has pores as narrow as MFI (10- membered ring). Unfortunately, other intermediates can also contribute to the bands close to this wavenumber.
To conclude the issue of DFT, the computational study predicts that the presence of DFM in the zeolite structure yields the band at the diagnostic wavenumber for DFM in the case of MOR and BEA, but it cannot be reasoned in a reverse
way, that is, that the band at ca. 1455 cm−1 can be a proof for
the presence of DFM.
Taking into account the modeling and experimental results, at least some contribution of the intermolecular mechanism of xylene isomerization is highly likely in MOR and BEA zeolites. In an intermolecular reaction, however, one intermediate molecule is formed for every two consumed, so generally intramolecular reactions are more entropically favored (conﬁgurational entropy). Moreover, it should be emphasized that the possibility of an intermolecular mechanism does not preclude the participation of the intramolecular one.
Impact of Aluminum Presence. For the structures with a
higher Si/Al ratio, the isomerization is less eﬀective, and the transalkylation rather takes place, particularly on the outer surface of the grain. The sorption energies for the xylene isomers in both silicalites and zeolites with ﬁnite Si/Al are summarized in Table 7. In silicalites, the sorption energy rises in the sequence of BEA < CHA < MOR < MFI. In the aluminated forms, however, the sequence generally is less monotonous with 12-MR BEA presenting the weakest sorption, except p-xylene, where the sorption energy is
postulated. Indeed, MOR and BEA structures (with 12-ring
channels) with DFM are energetically favoredall adsorption energies are negative (Table 6). Even DFM as a product is stable in all structures; the formation of DFM could be suppressed spatially in the zeolite with 10-ring channels.
Table 6. Sorption Energy (ΔEads), Gibbs Free Energy (ΔGads), and Description of Diagnostic IR Bands for DFM in Selected Zeolitesa
−42
−40
−53
−54
1456 (s)
−45
−42
1459
(vw)
1488 (w)
−59
−63
−69
*
1454
ΔE /(kcal/mol)
ads
ΔGads/(kcal/mol)
ν̃close to
1455 cm−1
scissoring
1455
(w)
3041 (s)
1472
(m)
2981 (s)
1457
(vs)
2966 (s)
1453
ν(̃CH2)/cm−1
stretching
ν(̃CH2)/cm
2919 (s)
2956
(s)
3000
(a)
−1
3133
(a)
3024 (a)
3005 (a)
3006 (a)
aThe labels “s”, “m”, “w”, “vs”, and “vw” denote strong, medium, weak, very strong, and very weak band intensity, respectively. Bands at
ca. 1455 cm−1 are in boldface. In the case of TNU, the intensities have
not been calculated. For stretching wavenumbers, the label “a” means asymmetric and “s” denotes symmetric vibrations.
Table 7. Sorption Free Enthalpy of Xylenes in Silicalites and Zeolites with Finite Si/Ala
∞
ΔGads/(kcal/mol)
−16
−15
−32
3
Si/Al
The scissoring vibration of CH at 1455 cm−1 is a diagnostic
−27
−21
−31
15
−21
−6
−15
−26
15
2
band of DFM. Vibrational analysis reveals the presence of the CH2 band in the range between 1455 and 1488 cm−1 (Table 6). This band turned out to be relatively weak except for the
case of BEA. Surprisingly, for MOR, another strong band appears at ca. 1455 cm−1, stemming from the asymmetric vibration of the benzene ring, but it is not the case for MFI (it appears at 1439(m) cm−1) or CHA (1459(vw) cm−1). Based on this observation, it can be concluded that if the diagnostic
band is present in the registered spectrum, it is the potential indication of the DFM presence, but the band in this region
ortho Meta Para Si/Al
−20
−35
8.6
ΔGads/(kcal/mol)
−30 (−9)	−28 (−12)
−20 (7)
−34 (−13)
−42 (−11)
−9 (−3)
−8 (7)
−33 (−7)
ortho meta para
−23 (−3)
−44 (−9)
−20 (−5)
−38 (−6)
aThe energy diﬀerence imposed by the introduction of Al is given in the parentheses.
10344
https://doi.org/10.1021/acs.jpcc.1c01307
J. Phys. Chem. C 2021, 125, 10334−10348
zeolite	MFI	MOR	CHA	BEA
MFI	MOR	CHA	BEA	TNU

The Journal of Physical Chemistry C
pubs.acs.org/JPCC
Article
comparable to that of other zeolites. In silicalites, the sorption is strongest for p-xylene, while m- and o-xylenes give similar sorption energy with exception of wide-channel BEA where sorption of o-xylene is very weak.
to the approximation used: the change in the dipole moment, calculated within the Hirshfeld population analysis, upon atomic displacement, used for the calculation of the dipolar transition moment.
In addition to the IR spectra, the adsorption energy of xylenes on silicalite and aluminated zeolites was also obtained. It was found that the protonated forms of xylenes (5- and 7- membered ring) are stabilized in zeolites.
The information concerning the structure of an intermediate
The aluminated zeolites have higher sorption energy for the
xylene of prolate molecular shapethe p-xylene molecule. The
wide-channel zeolite, BEA, has the strong sorption only for p-
xylene; for the other isomers, the sorption is weakin the former case (para), the methyl groups can come in a closer contact with walls of the channels, optimal from the point of view of the dispersion interactions. The o- and m-isomer molecules locate with the aromatic ring plane along the channel axis, and even in such an orientation, the protruding methyl groups cannot get closer to the channel walls. For other zeolites, the sorption is also the strongest for p-xylene compared to that for m- and o-xylene, although the diﬀerences are less pronounced. It seems, therefore, that the conﬁnement eﬀect is more decisive than the diﬀerence in xylene isomer basicity.
Generally, the introduction of Al in the zeolite structure strengthens sorption; only for m-xylene in BEA, it is weaker but only by 7 kcal/mol and is also weaker for o-xylene in MFI by 7 kcal/mol. Sorption of p-xylene is the strongest for all zeolites, while o- and m-xylenes yield values more diﬀerentiated than in the case of silicalites.
Considering two isomerization mechanisms, the intra- or intermolecular, the former is possible in all studied zeolites, while for the latter, the pore size has the dominant impact. The intermolecular mechanism of xylene isomerization is favored in the large-pore MOR and BEA zeolites. The formation of dicyclic aromatic intermediates was postulated for m-xylene isomerization.14,16 It was found that the reaction can be realized according to the intermolecular mechanism in medium-pore zeolites (with 10-ring channels), if they contain large internal cavities (FAU) or channel intersections (TNU-9, BEA) and in large-pore aluminosilicates (MCM-41). Taking into account that the CHA structure was chosen only as an epitome of the structure with a strong conﬁnement eﬀect, MFI is the zeolite which stabilizes the intermediates C5o (and C7-
in the intramolecular mechanism can be summarized in two
branches: the experimentalan intermediate of xylene
isomerization exhibits the IR band at 1485 cm−1, regardless
of the zeolite structure, and the DFT-basedthe total of 18 possible structures of protonated xylenes embedded in four
zeolites were modeled (ca. 70 systems). The band close to 1485 cm−1 appears in the calculated spectra for 13 out of 16 structures embedded in ZSM-5 zeolite. It was also found that
the energy of the intermediate formation depends on the zeolite deprotonation energy, ΔEdp, the stability of the intermediate itself, ΔEpr, and the energy of the zeolite− intermediate interaction, ΔEint.
Based on the spectroscopic results corroborated by the quantum chemical calculations, the following candidates for the intermediates can be postulated (Table 8):
Table 8. Candidates for the Intermediates in the Xylene Isomerization Reactions in MFI, MOR, CHA, and BEA Zeolitesa
C5o
y
s
y
u
y
s
y
s
C7-12
y
s
n
u
y
u
n
u
aνm̃atchwavenumber matching (yes/no). Estabstabilization energy:
negative (stable, “s”) or close to zero (“u”).

Note that the y/n ﬂags in the νm̃atch column mean that the diﬀerence between the experimental wavenumber and the simulated one was found not to be exceeding 10 cm−1.
The stability of the C5o intermediate in the small-pore zeolites changes in the following relationship: CHA ≃ MFI > BEA ≃ MOR; the same order is preserved for the concentration of the intermediates.
It can hence be concluded that the OH group acid strength is not a determining factor for the reactivity toward xylene isomerization. More emphasis should be placed on the availability of the OH groups to the diﬀusing o-xylene molecule (readiness for the formation of the transition structure), the energetics of the intermediate product, and the interaction of the o-xylene and transition structure with the host framework.
The xylenium ions (the 1485 cm−1 band) can therefore be
considered as the intermediate species both in the xylene isomerization and ETH process. The formation of protonated xylenes of the respective type and their further transformation through the intra- or intermolecular mechanism are ruled by the size of the internal voids of the zeolite structure. Consequently, the identiﬁcation of the intermediate products allows us to refer them the respective mechanisms and enables the design of a catalyst for the ETH process characterized by a high selectivity to p-xylene.

https://doi.org/10.1021/acs.jpcc.1c01307
J. Phys. Chem. C 2021, 125, 10334−10348
12 for the other reaction pathway) most strongly.
■
CONCLUSIONS
This work is aimed at providing the spectroscopic
and
theoretical insight into the intermediates formed according
to the hydrocarbon pool mechanism, which is considered as the main path in the alcohol transformation to higher hydrocarbons. Protonation and methyl-shift processes are deeply investigated in this work since the intermediates related to aromatic ring contraction and its expansion are widely proposed in the literature.
The experimental and computed spectra were compared, and a very good agreement was found in the wavenumbers of the diagnostic bands. The inﬂuence of the host on the electronic structure of xylene molecules was conﬁrmed
cm−1
computationally. The presence of the diagnostic 1485
band was also found for the intermediate structures (protonated 5- and 7-membered ring cations stemming from xylenes). The IR and computational study equivocally showed that the intermediates are more stable in zeolites with narrower
channels. Accuracy of the calculation was suﬃcient to attribute the experimentally observed diagnostic bands. The wave- numbers are reproduced with high accuracy, without scaling. The intensities, however, are not always well reproduced due
10345
MFI	MOR	CHA
νm̃atch	Estab	ν̃match	Estab	ν̃match	Estab
BEA
ν̃match	Estab

The Journal of Physical Chemistry C
pubs.acs.org/JPCC
Article
To brieﬂy recapitulate the article, the following highlights are summarized here:
main
Llopis, F.; Sastre, G.; Corma, A. Isomerization and disproportionation of m-xylene in a zeolite with 9- and 10-membered ring pores: Molecular dynamics and catalytic studies. J. Catal. 2006,
242, 195−206.
Belhekar, A. A.; Ahedi, R. K.; Kuriyavar, S.; Shevade, S. S.; Rao,
B. S.; Anand, R.; Tvaruzkova, Z. Effect of acid sites of Al- and Fe- Ferrierite on m-xylene isomerization. Catal. Commun. 2003, 4, 295− 302.
1. Pérez-Pariente, J.; Sastre, E.; Fornés, V.; Martens, J. A.; Jacobs, P. A.; Corma, A. Isomerization and disproportionation of m-xylene over zeolite β. Appl. Catal. 1991, 69, 125−137.
2. Corma, A.; Sastre, E. Evidence for a bimolecular isomerization of
xylenes on some large pore zeolites. J. Chem. Soc., Chem. Commun.
1991, 594−596.
1. Zheng, S.; Jentys, A.; Lercher, J. Xylene isomerization with surface-modified HZSM-5 zeolite catalysts: An in situ IR study. J. Catal. 2006, 241, 304−311.
2. Mirth, G.; Lercher, J. A. In Situ IR spectroscopic study of the
surface species during methylation of toluene over HZSM-5. J. Catal.
1991, 132, 244−252.
1. Mirth, G.; Cejka, J.; Lercher, J. A. Transport and isomerization of xylenes over HZSM-5 zeolites. J. Catal. 1993, 139, 24−33.
2. Mirth, G.; Lercher, J. A. On the Role of Product Isomerization
for Shape Selective Toluene Methylation over HZSM5. J. Catal. 1994,
147, 199−206.
Min, H.-K.; Cha, S. H.; Hong, S. B. Mechanistic insights into
the zeolite-catalyzed isomerization and disproportionation of m- xylene. ACS Catal. 2012, 2, 971−981.
Gołąbek, K.; Tarach, K. A.; Góra-Marek, K. Standard and rapid
scan infrared spectroscopic studies of o-xylene transformations in terms of pore arrangement of 10-ring zeolites − 2D COS analysis. Dalton Trans. 2017, 46, 9934−9950.
Gołąbek, K.; Tarach, K. A.; Góra-Marek, K. 2D COS analysis of
1. xylene transformation over medium-pore zeolites. Microporous Mesoporous Mater. 2018, 266, 90−101.
  1. Gołąbek, K.; Tarach, K. A.; Filek, U.; Góra-Marek, K. Ethylene
formation by dehydration of ethanol over medium pore zeolites.
Spectrochim. Acta, Part A 2018, 192, 464−472.
  1. Gołąbek, K.; Tarach, K. A.; Góra-Marek, K. Xylenes
transformation over zeolites ZSM-5 ruled by acidic properties.
Spectrochim. Acta, Part A 2018, 192, 361−367.
  1. Goguen, P. W.; Xu, T.; Barich, D. H.; Skloss, T. W.; Song, W.;
Wang, Z.; Nicholas, J. B.; Haw, J. F. Pulse-Quench catalytic reactor studies reveal a carbon-pool mechanism in Methanol-to-Gasoline chemistry on zeolite HZSM-5. J. Am. Chem. Soc. 1998, 120, 2650− 2651.
  1. Niu, X.; Wang, K.; Bai, Y.; Du, Y.-e.; Chen, Y.; Dong, M.; Fan,
W. Selective formation of para-xylene by methanol aromatization over phosphorous modified ZSM-5 zeolites. Catalysts 2020, 10, 484.
Olsbye, U.; Svelle, S.; Bjørgen, M.; Beato, P.; Janssens, T. V. W.; Joensen, F.; Bordiga, S.; Lillerud, K. P. Conversion of methanol to
hydrocarbons: how zeolite cavity and pore size controls product selectivity. Angew. Chem., Int. Ed. 2012, 51, 5810−5831.
Derouane, E.; Nagy, J. B.; Dejaifve, P.; van Hooff, J. H. C.;
Spekman, B. P.; Védrine, J. C.; Naccache, C. Elucidation of the mechanism of conversion of methanol and ethanol to hydrocarbons on a new type of synthetic zeolite. J. Catal. 1978, 53, 40−55.
1. Sun, J.; Wang, Y. Recent advances in catalytic conversion of ethanol to chemicals. ACS Catal. 2014, 4, 1078−1090.
2. van der Borght, K.; Batchu, R.; Galvita, V. V.; Alexopoulos, K.;
Reyniers, M.-F.; Thybaut, J. W.; Marin, G. B. Insights into the reaction mechanism of ethanol conversion into hydrocarbons on H- ZSM-5. Angew. Chem., Int. Ed. 2016, 55, 12817−12821.
Johansson, R.; Hruby, S. L.; Rass-Hansen, J.; Christensen, C. H.
The hydrocarbon pool in ethanol-to-gasoline over HZSM-5 catalysts.
Catal. Lett. 2009, 127, 1−6.
Kolboe, S. On the mechanism of hydrocarbon formation from methanol over protonated zeolites. Stud. Surf. Sci. Catal. 1988, 36, 189−193.
https://doi.org/10.1021/acs.jpcc.1c01307
J. Phys. Chem. C 2021, 125, 10334−10348
•
The availability of the OH groups allowing for the o- xylene molecules to form the TS seems more important for the reactivity in the xylene isomerization than the OH acid strength.
The other crucial factors are the energetics of the intermediates and the energetics of the o-xylene (and the formed transition structures) with the zeolite framework. Indeed, the smaller the cavity formed by intersecting channels (BEA, MOR, and MFI) or cages (CHA), the
higher the intensity of the 1485 cm−1 band detected in
the IR spectra.
•
■
AUTHOR INFORMATION
Corresponding Author
Witold Piskorz − Faculty of Chemistry, Jagiellonian University in Kraków, 30-387 Kraków, Poland;	orcid.org/0000- 0002-3462-436X; Email: wpiskorz@chemia.uj.edu.pl
Authors
Gabriela Jajko − Faculty of Chemistry, Jagiellonian University in Kraków, 30-387 Kraków, Poland;	orcid.org/0000- 0001-8286-917X
Karolina Tarach − Faculty of Chemistry, Jagiellonian University in Kraków, 30-387 Kraków, Poland;
orcid.org/0000-0003-0133-4363
Kinga Góra-Marek − Faculty of Chemistry, Jagiellonian University in Kraków, 30-387 Kraków, Poland;
orcid.org/0000-0002-1296-9244
Paweł Kozyra − Faculty of Chemistry, Jagiellonian University in Kraków, 30-387 Kraków, Poland;	orcid.org/0000- 0002-7168-5022
Complete contact information is available at: https://pubs.acs.org/10.1021/acs.jpcc.1c01307
Notes
The authors declare no competing ﬁnancial interest.
■
ACKNOWLEDGMENTS
The present study was funded by the National Science Centre of Poland (grant 2016/23/B/ST4/00088). Some of the calculations were performed in the Cyfronet PL-Grid super- computer center in Kraków, Poland. This work was partially
ﬁnanced by the National Science Centre of Poland (grant
2020/37/B/ST4/01215).
■
REFERENCES
(1) Zeolites in Industrial Separation and Catalysis; Kulprathipanja, S.,
Ed.; Wiley-VCH Verlag GmbH, 2010.
(2) Guisnet, M.; Gilson, J.-P. Zeolites for Cleaner Technologies;
Catalytic Science Series; Imperial Ccollege Press, 2002; Vol. 3.
(3) Chen, N. Y.; Degnan, T. F.; Smith, C. M. Molecular Transport
and Reaction in Zeolites: Design and Application of Shape Selective Catalysis; Springer, 1994.
Henriques, C. A.; Monteiro, J. L. F.; Magnoux, P.; Guisnet, M. Characterization of the Coke Formed Duringo-Xylene Isomerization over Mordenites at Various Temperatures. J. Catal. 1997, 172, 436−
445.
Li, Y.-G.; Jun, H. Kinetics study of the isomerization of xylene on ZSM-5 zeolites: the effect of the modification with MgO and CaO. Appl. Catal., A 1996, 142, 123−137.
10346

The Journal of Physical Chemistry C
pubs.acs.org/JPCC
Article
1. Dahl, I. M.; Kolboe, S. On the reaction mechanism for propene formation in the MTO reaction over SAPO-34. Catal. Lett. 1993, 20, 329−336.
2. Dahl, I. M.; Kolboe, S. On the reaction mechanism for
hydrocarbon formation from methanol over SAPO-34: 1. Isotopic labeling studies of the Co-reaction of ethene and methanol. J. Catal. 1994, 149, 458−464.
Dahl, I. M.; Kolboe, S. On the reaction mechanism for
hydrocarbon formation from methanol over SAPO-34: 2. Isotopic labeling studies of the Co-reaction of propene and methanol. J. Catal. 1996, 161, 304−309.
Costa, E.; Uguina, A.; Aguado, J.; Hernandez, P. J. Ethanol to
gasoline process: effect of variables, mechanism, and kinetics. Ind. Eng. Chem. Proc. Des. Dev. 1985, 24, 239−244.
Talukdar, A. K.; Bhattacharyya, K. G.; Sivasanker, S. HZSM-5
catalysed conversion of aqueous ethanol to hydrocarbons. Appl. Catal., A 1997, 148, 357−371.
1. Schulz, J.; Bandermann, F. Conversion of ethanol over zeolite H-ZSM-5. Chem. Eng. Technol. 1994, 17, 179−186.
2. Svelle, S.; Kolboe, S.; Swang, O.; Olsbye, U. Methylation of
alkenes and methylbenzenes by dimethyl ether or methanol on acidic zeolites. J. Phys. Chem. B 2005, 109, 12874−12878.
1. Mole, T.; Whiteside, J. A.; Seddon, D. Aromatic co-catalysis of methanol conversion over zeolite catalysts. J. Catal. 1983, 82, 261− 266.
2. Mole, T.; Bett, G.; Seddon, D. Conversion of methanol to hydrocarbons over ZSM-5 zeolite: An examination of the role of aromatic hydrocarbons using 13carbon- and deuterium-labeled feeds.
J. Catal. 1983, 84, 435−445.
Noda, I. Generalized two-dimensional correlation method
applicable to infrared, Raman, and other types of spectroscopy. Appl. Spectrosc. 1993, 47, 1329−1336.
Sadowska, K.; Góra-Marek, K.; Datka, J. Hierarchic zeolites
studied by IR spectroscopy: Acid properties of zeolite ZSM-5 desilicated with NaOH and NaOH/tetrabutylamine hydroxide. Vib. Spectrosc. 2012, 63, 418−425.
1. Datka, J.; Góra-Marek, K. IR studies of the formation of ammonia dimers in zeolites TON. Catal. Today 2006, 114, 205−210.
2. Delley, B. From molecules to solids with the DMol3 approach.
J. Chem. Phys. 2000, 113, 7756−7764.
1. Perdew, J. P.; Burke, K.; Ernzerhof, M. Generalized gradient approximation made simple. Phys. Rev. Lett. 1996, 77, 3865−3868.
2. Hammer, B.; Hansen, L. B.; Nørskov, J. K. Improved
adsorption energetics within density-functional theory using Per- dew-Burke-Ernzerhof functionals. Phys. Rev. B: Condens. Matter Mater. Phys. 1999, 59, 7413−7421.
Delley, B. Hardness conserving semilocal pseudopotentials.
Phys. Rev. B: Condens. Matter Mater. Phys. 2002, 66, 155125.
Benco, L.; Hafner, J.; Hutschka, F.; Toulhoat, H. Physisorption and chemisorption of some n-hydrocarbons at the Brønsted acid site in zeolites 12-membered ring main channels: ab initio study of the
gmelinite structure. J. Phys. Chem. B 2003, 107, 9756−9762.
Göltl, F.; Hafner, J. Modelling the adsorption of short alkanes
in protonated chabazite: The impact of dispersion forces and temperature. Microporous Mesoporous Mater. 2013, 166, 176−184.
Tkatchenko, A.; Scheffler, M. Accurate molecular van der Waals
interactions from ground-state electron density and free-atom reference data. Phys. Rev. Lett. 2009, 102, 073005.
1. Murnaghan, F. D. The compressibility of media under extreme pressures. Proc. Natl. Acad. Sci. U.S.A. 1944, 30, 244−247.
2. Fischer, T. H.; Almlof, J. General methods for geometry and wave function optimization. J. Phys. Chem. 1992, 96, 9768−9774.
3. Fletcher, R. Practical Methods of Optimization, 2nd ed.;
Springer: New York, N.Y., 1980; Vol. 1: unconstrained optimization.
Halgren, T. A.; Lipscomb, W. N. The synchronous-transit method for determining reaction pathways and locating molecular transition states. Chem. Phys. Lett. 1977, 49, 225−232.
1. Broyden, C. G. The convergence of a class of double-rank minimization algorithms 1. General considerations. IMA J. Appl. Math. 1970, 6, 76−90.
2. Hirshfeld, F. L. Bonded-atom fragments for describing molecular charge densities. Theor. Chim. 1977, 44, 129−138.
3. Mayer, I. Charge, bond order and valence in the ab initio SCF theory. Chem. Phys. Lett. 1983, 97, 270−274.
4. Sazama, P.; Tabor, E.; Klein, P.; Wichterlova, B.; Sklenak, S.;
Mokrzycki, L.; Pashkkova, V.; Ogura, M.; Dedecek, J. Al-rich beta zeolites. Distribution of Al atoms in the framework and related protonic and metal-ion species. J. Catal. Catalysis 2016, 333, 102− 114.
1. van Bokhoven, J. A.; Lamberti, C. Structure of aluminum, iron, and other heteroatoms in zeolites by X-ray absorption spectroscopy. Coord. Chem. Rev. 2014, 277−278, 275−290.
2. Olson, D. H.; Khosrovani, N.; Peters, A. W.; Toby, B. H.
Crystal structure of dehydrated CsZSM-5 (5.8Al): Evidence for nonrandom aluminum distribution. J. Phys. Chem. B 2000, 104, 4844−4848.
Akporiaye, D. E.; Dahl, I. M.; Mostad, H. B.; Wendelbo, R.
Aluminum distribution in chabazite: An experimental and computa- tional study. J. Phys. Chem. 1996, 100, 4148−4153.
Oumi, Y.; Kanai, T.; Lu, B.; Sano, T. Structural and physico-
chemical properties of high-silica mordenite. Microporous Mesoporous Mater. 2007, 101, 127−133.
Karcz, R.; Dedecek, J.; Supronowicz, B.; Thomas, H. M.; Klein,
P.; Tabor, E.; Sazama, P.; Pashkova, V.; Sklenak, S. TNU-9 zeolite:
aluminum distribution and extra-framework sites of divalent cations.
Chem.Eur. J. 2017, 23, 8857−8870.
1. Pine, L.; Maher, P. J.; Wachter, W. A. Prediction of cracking catalyst behavior by a zeolite unit cell size model. J. Catal. 1984, 85, 466−476.
2. Al-Khattaf, S.; Ali, S. A.; Aitani, A. M.; Žilková, N.; Kubicǩa, D.;
Čejka, J. Recent advances in reactions of alkylbenzenes over novel
zeolites: the effects of zeolite structure and morphology. Catal. Rev.
2014, 56, 333−402.
1. Boronat, M.; Corma, A. What is measured when measuring acidity in zeolites with probe molecules? ACS Catal. 2019, 9, 1539− 1548.
2. Derouane, E.; Andre, J.-M.; Lucas, A. A. Surface curvature effects in physisorption and catalysis by microporous solids and molecular sieves. J. Catal. 1988, 110, 58−73.
3. Derouane, E. G. Zeolites as solid solvents. J. Mol. Catal. A: Chem. 1998, 134, 29−45.
4. Deshlahra, P.; Iglesia, E. Reactivity descriptors in acid catalysis: acid strength, proton affinity and host−guest interactions. Chem. Commun. 2020, 56, 7371−7398.
5. Mangold, M.; Rolland, L.; Costanzo, F.; Sprik, M.; Sulpizi, M.;
Blumberger, J. Absolute pK a values and solvation structure of amino acids from density functional based molecular dynamics simulation. J. Chem. Theory Comput. 2011, 7, 1951−1961.
Lee, C.; Parrillo, D. J.; Gorte, R. J.; Farneth, W. E. Relationship
between differential heats of adsorption and Brønsted acid strengths of acidic zeolites: H-ZSM-5 and H-Mordenite. J. Am. Chem. Soc. 1996, 118, 3262−3268.
Parrillo, D. J.; Lee, C.; Gorte, R. J. Heats of adsorption for
ammonia and pyridine in H-ZSM-5: evidence for identical Brønsted- acid sites. Appl. Catal., A 1994, 110, 67−74.
Tsutsumi, K.; Nishimiya, K. Differential molar heats of
adsorption of ammonia on silicious mordenites at high temperature.
Thermochim. Acta 1989, 143, 299−309.
Suzuki, K.; Sastre, G.; Katada, N.; Niwa, M. Periodic DFT
calculation of the energy of ammonia adsorption on zeolite Brønsted acid sites to support the ammonia IRMS−TPD Experiment. Chem. Lett. 2009, 38, 354−355.
Nachtigallová, D.; Bludsky,́O.; Otero Areán, C.; Bulánek, R.;
Nachtigall, P. The vibrational dynamics of carbon monoxide in a confined space - CO in zeolites. Phys. Chem. Chem. Phys. 2006, 8, 4849−4852.
https://doi.org/10.1021/acs.jpcc.1c01307
J. Phys. Chem. C 2021, 125, 10334−10348
10347

The Journal of Physical Chemistry C
pubs.acs.org/JPCC
Article
1. Gutsev, G. L.; Boldyrev, A. I. DVM-Xα calculations on the ionization potentials of complex anions and the electron affinities of MXk+1 “superhalogens”. Chem. Phys. 1981, 56, 277−283.
2. Czapla, M.; Skurski, P. Toward the preparation of the HAuF6,
HAu2F11, and HAu3F16 superacids: Theoretical study. Int. J. Quantum Chem. 2018, 118, No. e25494.
10348
https://doi.org/10.1021/acs.jpcc.1c01307
J. Phys. Chem. C 2021, 125, 10334−10348