Hindawi
Journal of Analytical Methods in Chemistry Volume 2018, Article ID 3587860, 8 pages https://doi.org/10.1155/2018/3587860
Research Article
The Potential of Graphene as an Adsorbent for Five Pesticides from Different Classes in Rape Oil Samples Using Dispersive
Solid-Phase Extraction
Katarzyna Madej,1 Katarzyna Janiga,1 and Wojciech Piekoszewski
1,2
1Department of Analytical Chemistry, Faculty of Chemistry, Jagiellonian University, Krakow 30-387, Poland
2Department of Food Science and Technology, School of Biomedicine, Far Eastern Federal University, Vladivostok, Russia
Correspondence should be addressed to Wojciech Piekoszewski; wpiekosz@tlen.pl
Received 15 September 2017; Revised 1 January 2018; Accepted 11 January 2018; Published 1 April 2018
Academic Editor: Mohamed Abdel-Rehim
Copyright © 2018 Katarzyna Madej et al. This is an open access article distributed under the Creative Commons Attribution License, which permits unrestricted use, distribution, and reproduction in any medium, provided the original work is properly cited.
Isolation conditions for ﬁve pesticides (metazachlor, tebuconazole, λ-cyhalothrin, chlorpyrifos, and deltamethrin) from rape oil samples were examined using the dispersive solid-phase graphene extraction technique. To determine the optimal ex- traction conditions, a number of experimental factors (amount of graphene, amount of salt, type and volume of the desorbing solvent, desorption time with and without sonication energy, and temperature during desorption) were studied. The com- pounds of interest were separated and detected by an HPLC-UV employing a Kinetex XB-C18 column and a mobile phase consisting of acetonitrile and water ﬂowing in a gradient mode. The optimized extraction conditions were: the amount of graphene 15 mg, desorbing solvent (acetonitrile) 5 mL, time desorption 10 min at 40°C, and amount of NaCl 1 g. The detection
limit for metazachlor, tebuconazole, λ-cyhalothrin, and chlorpyrifos was 62.5 ng·g−1, and for deltamethrin, it was 500 ng·g−1.
The obtained results lead to the conclusion that graphene may be successfully used for the isolation of the ﬁve pesticides from rape oil. However, their determination at low concentration levels, as they occur in real oil samples, requires the employment of appropriately highly sensitive analytical methods, as well as a more suitable graphene form (e.g., magnetically modiﬁed graphene).
advanced coupled techniques as LC-MS/MS [1, 2], LC-TOF- MS [3], UHPLC-MS/MS [4, 5], GC-MS/MS [2, 6], and GC-MS
[7]. The employment of GC-ECD [8, 9], HPLC/UV [10], or HPLC/DAD [11] in this analytical area has also been reported. Generally, in all cases of oil matrix analysis, an appropriate sample preparation procedure, usually consisting of two or more stages, was required. In most cases, QuEChERS or modiﬁed QuEChERS-based procedures as the cleanup step were involved [1–6, 8]. In some cases, these were preceded by the freezing step for oil precipitation [2, 3, 8, 10]. The separate review article concerning recent developments and trends in the QuEChERS sample preparation approach, including the analysis of pesticides in various fatty food samples, was also presented [12].
1. Introduction
Due to the potential toxicity, bioaccumulating properties, and wide use of pesticides for supporting and intensiﬁcation of crops almost all over the world, these substances belong to the most often controlled ones in the environment and in food. Every year, many publications devoted to the devel- opment of new methods for pesticide determination in various food matrices appear. However, pesticide residue analysis in high-fat samples is still a challenging analytical task. Edible oil samples belong to such analytically diﬃcult matrices. Due to complex matrices, as well as low con- centrations of pesticide residues, frequently originated from various classes, these samples are analyzed using such

2
Journal of Analytical Methods in Chemistry
N+ N
O
H3C
CH3
CH3
Cl
N
N
HO
H3C
CH3
N+
N
Cl
log P = 2.7
log P = 3.7
(b)
(a)
F
F
O
F
Cl
Cl
Cl
O
S
CH3
O
P
Cl
N
O
CH3
N
O
H3C
O
CH3
log P = 6.1
(c)
log P = 4.95
(d)
Br
H3C
CH3
O
O
Br
O
N
log P = 6.2
(e)
Figure 1: Chemical structures of the
studied uve pesticides with their partition coeffi cients (log P).
Metazachlor (log P = 2.7) (a);
tebuconazole (log P = 3.7) (b); λ-cyhalothrin (log P = 6.1) (c); chlorpyrifos (log P = 4.95) (d); deltamethrin (log P = 6.2) (e).
Graphene is a carbon nanomaterial which has been widely used (especially in modiued forms) in de- termination of organic compounds including pesticides, usually in relatively simple matrices. rese include envi- ronmental waters [13–16], fruit juices [17], fruits [18],
vegetables [18–20], and teas [21, 22]. re potential unique adsorption properties of graphene resulted mainly from its large surface area and strong π-π interactions between its large delocalized electron system and the aromatic rings of the target molecules [23].
In this work, the main focus was to evaluate the ad- sorption potential of nonmodiued graphene for the isolation of selected pesticides from various groups (chloroacetamide herbicides, triazole fungicides, pyrethroids, and organo- phosphorus pesticides) present in rape oil samples, which are commonly used for supporting of rape crops. To our best knowledge, this is the urst time that graphene has been tried as the adsorbent for isolation of pesticides from such a diffi cult matrix as edible oil. re chemical structures of the studied components are presented in Figure 1.
Dispersive solid-phase extraction (d-SPE) combined with graphene was selected as the sample treatment method, and the HPLC-UV technique was used for the separation and detection of the compounds of interest in the resulting oil extracts.
1. Materials and Methods
  1. Preparation of Standard Samples and Graphene
Suspension. re stock of methanolic solutions of metaza-
−
chlor, tebuconazole, λ-cyhalothrin, chlorpyrifos, and delta-
−1)
methrin (1 mg·mL 1) and the internal standard chlorfenvinphos
(1 mg·mL
were stored in a refrigerator at 4°C. re
standard solutions were prepared by appropriate dilution
−1)
of the stock solutions with methanol. re graphene
suspension (3 mg·mL	was prepared by weighing an
appropriate amount of solid graphene and dispersing it in a suitable amount of deionized water using sonication for 6 h. re oil samples were prepared by weighing 1 gram of a commercial, ratiued rape oil and then spiking it with

Journal of Analytical Methods in Chemistry
3
appropriate amounts of standard solutions of the ﬁve or six pesticides and then left for equilibration at room temperature for one hour.
the method of one independent variable. The extraction
recovery (ER) for each pesticide was calculated from the
(1)
following equation:
P
pesticide in sample extract
ER(%) �
· f · f · 100,
1	2
2.2. Apparatus. For oil sample preparation, the following laboratory equipment was used: technical balance (Radwag WPX 250, Poland), vortex TK 35 (Techno-Kartel, Germany), centrifuge MPW-260R (DHN, Poland), thermoblock TB- 941U (Poland), and sonic bath Vibra Cell (Sonics & Ma- terials Inc., USA). Chromatographic analyses were per- formed using the chromatographic system (Merck-Hitachi LaChrom) consisting of an L-7100 pump and an L-7455 UV spectrophotometric detector (Darmastadt, Germany) equip-
Ppesticide standard
where Ppesticide in sample extract is the area of the peak corre- sponding to the pesticide in a sample extract, Ppesticide standard is the area of the peak corresponding to the pesticide in a standard solution, f1 is the ratio of theoretical volume of an acetonitrile supernatant above the frozen fat layer to volume
of an acetonitrile supernatant taken from above the frozen fat layer, f2 is the ratio of theoretical volume of an acetonitrile supernatant after desorption to volume of an acetonitrile supernatant after desorption, taken for evaporation.
For standardizing the extraction procedure, the aceto- nitrile supernatant volumes were taken to be the same, that is,
3.5 mL of the supernatant from above the frozen fat layer and 4 mL of the supernatant after the desorption process. Thus,
ped with a Kinetex XB-C18 column (150 × 4.6 mm, 5 µm)
which was supplied by Phenomenex (USA). The column temperature was 25°C. A mixture of water (A) and acetonitrile
(B) was used as the mobile phase. The following optimal gradient conditions of the mobile phase ﬂow were applied:
0 min (70% A and 30% B), 20 min (24% A and 76% B), 25 min
−
values of the coeﬃcients f1 and f2 are equaled to 1.14 and 1.25,
OC � 5 · ∑ ERi � maximum,
(0% A and 100% B), and 35 min (0% A and 100% B). The ﬂow
respectively. As the optimization criterion (OC), the maxi-
rate was 1 mL·min 1. The pesticides were detected at λ � 220 nm.
mum average recovery rate for the ﬁve pesticides was adopted:
(2)
The injection volume of standard solutions as well as oil sample extracts was 40 µL.
�
5
n
1
i�1
2.3. Generald-SPE(Graphene) Procedure. For initial isolation
minimum 2 h at −
of the ﬁve pesticides, 4 mL of acetonitrile was added with 1 g pesticide-spiked oil, vortexed (1 min), and left to freeze for
where i is the pesticide number and n � 5 is the number of
the studied pesticides.
32 C in a horizontal position. An acetonitrile
°
supernatant was decanted into a clean centrifuge test tube
(7 mL) from above the frozen fat layer. The supernatant was
3.1. Eﬀect of Graphene Suspension Volume. Graphene was used as an adsorbent for the ﬁve pesticides. This nano- structured material seems to be an excellent adsorbent due to its huge surface area, as well as the hexagonal arrays of carbon atoms that are suitable for strong interactions with organic molecules, especially those possessing aromatic rings in- cluding the pesticides. The very large delocalized π-electron
system enables the formation of strong π-π stacking in-
teractions with aromatic rings [23].
To reduce errors when adding graphene to samples and to make the operation easy, graphene was prepared in the form of aqueous suspension. The amount of graphene was optimized at the ﬁve volume levels of the graphene sus- pension: 3, 4, 5, 6, and 7 mL. The remaining conditions such as the mass of NaCl (2 g), type and volume of the desorbing solvent (4 mL), sonication, desorption time (10 min), and temperature (ambient) during the desorption process were left constant. From this optimization step, the extraction results are shown in Table 1.
The maximal average value of extraction recovery for the ﬁve compounds was obtained for 5 mL of aqueous graphene suspension, and this volume was used for further study.
evaporated to almost dryness, and then, an appropriate amount of aqueous graphene suspension and solid sodium chloride (for salting out pesticides) was added. The whole content of the test tube was vortexed (1 min) and then centrifuged (10 min, 14,000 rpm). Using a Pasteur pipette, the upper layer was discarded, and 4 mL of desorbing solvent was added to the bottom layer of graphene with the adsorbed pesticides and vortexed for 1 min without pre- vious sample heating or after increasing the sample temperature in a thermoblock. Subsequently, the sample was subjected to sonication for an appropriate time at an appropriate temperature. The content was centrifuged (10 min, 14,000 rpm), and the acetonitrile supernatant with desorbed compounds was successfully transferred into an Eppendorf tube (2 mL) and evaporated to dryness under
nitrogen in a thermoblock at 40°C. The dried residue was reconstituted into 200 µL of methanol and was ready for injection onto the chromatographic column.

3. Results
In order to obtain the best extraction conditions for isolation of the ﬁve studied pesticides from oil samples, several ex- perimental factors such as the volume of graphene sus- pension, amount of the salt (NaCl), type and volume of the desorbing solvent, desorption time with and without ap- plication of sonication energy, and desorption temperature were studied. The optimization process was conducted using
3.2. Eﬀect of Desorbing Solvent Type. Four diﬀerent solvents such as acetonitrile, acetone, ethyl acetate, and a mixture of n-hexane and dichloromethane (2 : 1, v/v) were tested as the desorbing agents for the studied pesticides from graphene. The choice of the tested solvents was based on their

4
Journal of Analytical Methods in Chemistry
Table 1: Eﬀect of the graphene amount on extraction eﬃcacy of the ﬁve pesticides from rape oil samples.
Extraction recovery (%), n � 3
11 ± 3
64 ± 7
26 ± 5
14 ± 5
Pesticide
9 mg of graphene
12 mg of graphene	15 mg of graphene	18 mg of graphene
21 mg of graphene
38 ± 8
72 ± 5
44 ± 7
29 ± 7
Metazachlor Tebuconazole λ-Cyhalothrin Chlorpyrifos Deltamethrin OC1
68 ± 5
77 ± 5
60 ± 5
66 ± 7
68 ± 9
67.0 ± 6.2
56 ± 7
52 ± 6
38 ± 11
17 ± 8
12 ± 7
63 ± 9
49 ± 7
23 ± 6
13 ± 5
63 ± 11
18 ± 4
14 ± 5
26.0 ± 20.3
63.0 ± 7.1
35.1 ± 12.6
19.4 ± 6.5
2
2
1Value of the optimization criterion; 2statistically signiﬁcant from the highest result.
Table 2: Eﬀect of the desorbing solvent type on extraction eﬃcacy of the ﬁve pesticides from rape oil samples.
Extraction recovery (%), n � 3
33 ± 5
61 ± 8
43 ± 6
Pesticide
Acetonitrile
Acetone
Ethyl acetate
Dichloromethane/hexane (1 : 2,v/v)
22 ± 5
25 ± 5
34 ± 8
Metazachlor Tebuconazole λ-Cyhalothrin Chlorpyrifos Deltamethrin OC1
68 ± 6
74 ± 7
60 ± 6
66 ± 6
66 ± 5
66.7 ± 5.0
20 ± 4
50 ± 6
42 ± 6
42 ± 3
8 ± 7
63 ± 6
21 ± 3
39 ± 5
34 ± 5
27.7 ± 9.5
36.9 ± 20.8
43.5 ± 11.8
2
2
2
1Value of the optimization criterion; 2statistically signiﬁcant from the highest result.
Table 3: Eﬀect of the desorbing solvent volume on extraction eﬃcacy of the ﬁve pesticides from rape oil samples.
Extraction recovery (%), n � 3
18 ± 4
54 ± 6
29 ± 8
15 ± 3
Pesticide
3 mL of acetonitrile
4 mL of acetonitrile	5 mL of acetonitrile	6 mL of acetonitrile
7 mL of acetonitrile
38 ± 5
70 ± 5
48 ± 6
29 ± 5
Metazachlor Tebuconazole λ-Cyhalothrin Chlorpyrifos Deltamethrin OC1
68 ± 6
76 ± 5
65 ± 5
69 ± 8
67 ± 6
69.2 ± 4.2
34 ± 6
54 ± 7
32 ± 9
16 ± 5
22 ± 6
61 ± 10
51 ± 5
25 ± 7
16 ± 4
21 ± 8
25.9 ± 9.8
59.8 ± 6.7
36.2 ± 12.9
19.7 ± 7.1
60 5
12 5
2
2
1Value of the optimization criterion; 2statistically signiﬁcant from the highest result.
the desorbing solvent on the extraction results of the ﬁve pesticides was examined. The remaining conditions of the volume of the graphene suspension (5 mL), amount of NaCl (2 g), type of the desorbing solvent (acetonitrile), soni- cation, desorption time (10 min), and temperature (am- bient) during desorption were left constant. The highest extraction recovery for all the analytes was obtained using 5 mL of acetonitrile, and this volume was used in further experiments. The eﬀect of this parameter is shown in Table 3.
polar/hydrophobic properties. The hydrophobicity of the solvents along with their elution strength in relation to the studied pesticides, adsorbed on graphene, increases in the following sequence: acetone, acetonitrile, ethyl acetate, and a mixture of n-hexane and dichloromethane (2 1, v/v). The remaining conditions of the volume of the graphene suspension (5 mL), amount of NaCl (2 g), volume of the desorbing solvent (4 mL), sonication, desorption time (10 min), and temperature (ambient) during desorption were left constant. Considering the ease of experimental opera- tions (very good separation of the organic supernatant and the graphene phase), the best solvent appeared to be ethyl acetate. The maximal extraction recovery for all of the pesticides was achieved with acetonitrile. Therefore, aceto- nitrile was selected as the desorbing solvent for further optimization process. The eﬀect of the type of the used solvent is shown in Table 2.
3.4. Eﬀect of Sonication Energy and Desorption Time. For desorbing the ﬁve pesticides from graphene, 5 mL of ace- tonitrile was added to the graphene phase (with the adsorbed analytes) at the bottom of a tube and vortexed for 1 min and then subjected to sonication energy for 5 and 10 minutes. Additionally, in a separate experiment, the graphene phase was vortexed (1 min) without applying sonication energy. The rest of the experimental conditions (volume of graphene suspension (5 mL) and ambient temperature during
3.3. Eﬀect of Desorbing Solvent Volume. The eﬀect of the ﬁve diﬀerent volumes of acetonitrile (3, 4, 5, 6, and 7 mL) as

Journal of Analytical Methods in Chemistry
5
Table 4: Eﬀect of the sonication energy and desorption time on extraction eﬃcacy of the ﬁve pesticides from rape oil samples.
Extraction recovery (%), n � 3
24 ± 4
37 ± 9
Pesticide
10 minutes subjected to sonication
5 minutes subjected to sonication
Without sonication energy
9 ± 4
43 ± 6
Metazachlor Tebuconazole λ-Cyhalothrin Chlorpyrifos Deltamethrin OC1
68 ± 8
74 ± 7
60 ± 7
66 ± 6
66 ± 7
67.0 ± 4.8
24 ± 7
32 ± 6
42 ± 8
63 ± 7
9 ± 5
10 ± 5
21.8 ± 3.7
37.0 ± 19.1
2
2
1Value of the optimization criterion; 2statistically signiﬁcant from the highest result.
Table 5: Eﬀect of the NaCl amount on extraction eﬃcacy of the ﬁve pesticides from rape oil samples.
Extraction recovery (%), n � 3
68 ± 5
22 ± 6
Pesticide
2 g NaCl
1 g NaCl
Without addition of NaCl
74 ± 8
19 ± 4
Metazachlor Tebuconazole λ-Cyhalothrin Chlorpyrifos Deltamethrin OC1
69 ± 6
73 ± 8
63 ± 4
70 ± 9
68 ± 7
68.5 ± 4.2
60 ± 7
9 ± 5
66 ± 7
24 ± 5
66 ± 7
20 ± 5
66.8 ± 5.5
19.0 ± 6.5
2
1Value of the optimization criterion; 2statistically signiﬁcant from the highest result.
Table 6: Eﬀect of the desorption temperature on extraction eﬃcacy of the ﬁve pesticides from rape oil samples.
Extraction recovery (%), n � 3
69 ± 10
Pesticide
At ambient temperature
At increased temperature (40°C)
74 ± 8
Metazachlor
81 ± 5
63 ± 5
Tebuconazole
84 ± 7
 ±
λ-Cyhalothrin
59 ± 5
68 ± 7
Chlorpyrifos
70 6
83 ± 5
56.0 ± 3.8
Deltamethrin
98 ± 8
OC1
2
80.9 ± 13.0
1Value of the optimization criterion; 2statistically signiﬁcant from the highest result.
desorption) were kept constant. A desorption process of 10 min gave the greatest extraction recovery. The eﬀects of these experiments on extraction results are given in Table 4.
desorption process from graphene. In the ﬁrst step, the graphene phase (with the adsorbed pesticides) was heated with 5 mL of acetonitrile in a thermoblock to a temperature of 40°C; in the second step, the content of the tube was subjected to sonication for 10 min, maintaining the tem- perature at 40°C. The rest of the experimental parameters (volume of graphene suspension (5 mL), acetonitrile volume (5 mL), and sonication (10 min)) were kept constant. The eﬀect of increasing the desorption temperature and how it considerably improves extraction eﬃciency are shown in Table 6.
3.5. Eﬀect of the Salt Added. In all the above experiments, before introduction of the graphene suspension to an oil sample, 2 g of NaCl was added for salting out of the pes- ticides. In this optimization step, the extraction eﬃcacy of the analytes was studied by decreasing the amount of salt added to 1 g or performing the sample preparation pro- cedure without addition of NaCl. The rest of the experi- mental parameters (volume of graphene suspension (5 mL), acetonitrile volume (5 mL), sonication (10 min), and am- bient temperature during desorption) were kept constant. The results are given in Table 5.
3.7. Evaluation of Linearity Rangeand Limit of Detection of the d-SPE (Graphene)-HPLC/UV Method. At the optimized extraction conditions, the linearity range and detection limit for each pesticide were determined.
Representative chromatograms are presented in Figure 2,
Calibration curves were designed on the basis of analyses of oil samples containing mixtures of the ﬁve pesticides at the
3.6. Eﬀect of Desorption Temperature. The ﬁnal experimental factor studied was the temperature of the pesticide

6
Journal of Analytical Methods in Chemistry
0.10
0.08
0.06
0.04
0.02
0.00
–0.02
0.10
0.08
0.06
0.04
0.02
0.00
–0.02
5
3
23
1
3
4
5
5
10
15
20
25
30
35
Retention time (min)
(a)
Retention time (min)
(b)
0.10

0.08

0.06

0.04
0.02

0.00
2
1
3
3 4
–0.02 0
5
10
15
20
25
30
35
Retention time (min)
(c)
Figure 2: Chromatograms of the extract of the blank rape oil sample (a), uve standard pesticides (1 µg/1 ml of methanol) (b), and the extract of the rape oil sample, spiked with the uve standard pesticides (c) (concentration (62.5 ng/g) equal to LOQ). 1: metazachlor; 2: tebuconazole; 3: λ-cyhalothrin; 4: chlorpyrifos; 5: deltamethrin.
−
−
1
six concentrations (62.5, 125, 250, 500, 1000, and 2000 ng·g )
solvent (acetonitrile), volume of the desorbing solvent (5 mL), desorption time using sonication energy (10 min), desorption temperature (40°C), and amount of salt (1 g NaCl). Under the optimized conditions, the following extraction recoveries for the examined pesticides were achieved: meta- zachlor (81%), tebuconazole (84%), λ-cyhalothrin (59%), chlorpyrifos (83%), and deltamethrin (98%). ris is the urst application of graphene-based materials in the analysis of pesticides in oil samples. rere are relatively a small number of reports of carbon nanomaterials being used to extract pesticides from other less-complicated matrices including metazachlor from surface waters [24]; tebuconazole from environmental water [25], vegetable [20], and tea [22] samples; λ-cyhalothrin and deltamethrin from fruit [26] and vegetable [26, 27] samples; and chlorpyrifos from envi- ronmental water [14] and tea samples [22]. Depending on the kind of the pesticide or/and pesticide concentration and type of a matrix, the extraction recoveries of the pesticides of interest ranged from 79.0 to ca. 100%. re pesticides were separated and detected using the RP chromatographic system, which was adopted from literature [11] with slight modiucations due to the tested pesticides. re detection limits of the uve pesticides determined by the d-SPE (graphene)-HPLC/UV method were not quite satisfactory
−1
and the internal standard (chlorfenvinphos, 1 µg·mL 1). A
linearity range 62.5–2000 ng·g	was achieved for meta-
zachlor, tebuconazole, λ-cyhalothrin, and chlorpyrifos
with determination coeffi cients (r2) 0.998, 0.991, 0.999, and
−1
0.993, respectively. For deltamethrin, the linearity range
was 500–2000 ng·g	with r2 = 0.999. re detection limit
was determined by estimation of the minimum concen-
tration as equivalent to three times the background noise
−1,
signal. re detection limit for metazachlor, tebuconazole,
−1.
λ-cyhalothrin, and chlorpyrifos was 62.5 ng·g	and for
deltamethrin, it was 500 ng·g
4. Discussion
re potential adsorption properties of simple nonmodiued graphene for the uve pesticides (metazachlor, tebuconazole, λ-cyhalothrin, chlorpyrifos, and deltamethrin) analyzed
acetonitrile and freezing at −32 C and (2) adsorption on the
from a rape oil matrix were explored. re fat content from
the matrix was removed at two stages: (1) precipitation with
°
graphene surface (a smaller amount of oil left in the ace-
tonitrile phase). re pesticides were adsorbed on graphene
because of its high speciuc surface area, as well as through noncovalent interactions, especially the π-π stacking in-

and the hydrophobic effect.
re optimized d-SPE (graphene) extraction conditions for the uve compounds present in rape oil samples were as follows: amount of graphene (15 mg), type of the desorbing
because some of them were above maximum residue levels
−1
−
(MRL = 0.07 mg·kg 1), metazachlor (MRL = 0.06 mg·kg ),
−1
−1
and chlorpyrifos (MRL = 0.05 mg·kg 1). For λ-cyhalothrin
(MRL = 0.2 mg·kg ) and tebuconazole (MRL = 0.5 mg·kg ),
the developed method may be used as the so-called “cutoff”
Absorbance
Absorbance
Absorbance

0	5	10	15	20	25	30	3

Journal of Analytical Methods in Chemistry
7
method allowing to separate “good” samples from “bad” oil samples. However, in our investigations, HPLC-UV, which is a relatively not highly sensitive technique, was primarily used as the detection tool for estimating the adsorption potential of graphene for the studied pesticides present in the oil matrix. In the abovementioned works, the detection limits achieved were considerably lower (single nanogram or less), but in the vast majority cases (with the exceptions of
[25] and [27] where 300 mL of the aqueous sample was analyzed by HPLC-UV and a 10 g portion of the homoge- nized plant sample was assayed by GC-ECD, resp.), highly sensitive detection methods like mass spectroscopy (MS) or tandem mass (MS-MS) spectroscopy were used.
Conclusion
In most cases of pesticide analysis involving graphene as an adsorbent, magnetic solid-phase extraction (MSPE) was applied where magnetically modiﬁed graphene composites as adsorbents were used. Only few works reported the employment of nonmodiﬁed graphene alone or in combi- nation with other sorbents (in the modiﬁed QuEChERS method) using dispersive solid-phase extraction. This is the ﬁrst time when graphene in its nonmodiﬁed form, using d-SPE, was studied as the adsorbent for the pesticides from four diﬀerent groups present in such analytically diﬃcult matrices as edible oil. Graphene may be successfully exploited in the preparation of edible oil samples for determination of pesticides from various groups. However, some improvements should be introduced in such analyses. For example, a more sensitive analytical method (e.g., GC-MS or LC-MS) may be used. Additionally, a more suitable modiﬁed graphene form, for example, magnetically modiﬁed graphene, which will prevent the nanomaterial aggregation, increase its disper- sion in solvents, and improve its adsorption properties, would better enable separation of graphene from the isolated analytes in the supernatant using an external magnet.
Conflicts of Interest
The authors declare that they have no conﬂicts of interest.
References
  1. L. Polga´r, B. Kmella´r, J. F. Garc´ıa-Reyes, and P. Fodor, “Comprehensive evaluation of the clean-up step in QuEChERS procedure for the multi-residue determination of pesticides in diﬀerent vegetable oils using LC-MS/MS,” Analytical Methods, vol. 4, no. 4, p. 1142, 2012.
  2. C. Anagnostopoulos and G. E. Miliadis, “Development and validation of an easy multiresidue method for the determination of multiclass pesticide residues using GC-MS/MS and LC- MS/MS in olive oil and olives,” Talanta, vol. 112, pp. 1–10, 2013.
  3. E. Sobhanzadeh, N. K. A. Bakar, A. M. R. Bin, and K. Nemati,
“A simple and eﬃcient multi-residue method based on QuEChERS for pesticides determination in palm oil by liquid chromatography time-of-ﬂight mass spectrometry,” Environmental Monitoring and Assessment, vol. 184, no. 9, pp. 5821–5828, 2012.
  1. D. Moreno-Gonza´lez, J. F. Huertas-Pe´rez, A. M. Garc´ıa-Campaña, and L. Ga´miz-Gracia, “Determination of carbamates in edible
vegetable oils by ultra-high performance liquid chromatography- tandem mass spectrometry using a new clean-up based on zirconia for QuEChERS methodology,” Talanta, vol. 128, pp. 299–304, 2014.
O. Lacina, M. Zachariasova, J. Urbanova, M. Vaclavikova,
T. Cajka, and J. Hajslova, “Critical assessment of extraction methods for the simultaneous determination of pesticide residues and mycotoxins in fruits, cereals, spices and oil seeds employing ultra-high performance liquid chromatography– tandem mass spectrometry,” Journal of Chromatography A, vol. 1262, pp. 8–18, 2012.
P. Deme, T. Azmeera, B. L. A. P. Devi, P. R. Jonnalagadda,
R. B. N. Prasad, and U. V. R. Vijaya Sarathi, “An improved dispersive solid-phase extraction clean-up method for the gas chromatography – negative chemical ionisation tandem mass spectrometric determination of multiclass pesticide residues in edible oils,” Food Chemistry, vol. 142, pp. 144–151, 2014.
T. Liu, Y. Ren, J. Xie, G. Song, and Y. Hu, “Determination of organophosphorus pesticides in edible oils by dispersive microextraction based on acetonitrile/water-coated Fe3O4,” Journal of the American Oil Chemists’ Society, vol. 90, no. 12, pp. 1937–1943, 2013.
termination of λ-cyhalothrin and cypermethrin in palm oil
[8] H. Muhamad, B. Hisyam, N. Kartini, and A. Bakar, “Com-
parative study of diﬀerent clean-up techniques for the de-
matrices by gas chromatography with electron capture de-
tection,” Food Chemistry, vol. 134, no. 4, pp. 2489–2496, 2012.
[9] J. Li, D. Liu, T. Wu, W. Zhao, Z. Zhou, and P. Wang, “A
simpliﬁed procedure for the determination of organochlorine pesticides and polychlorobiphenyls in edible vegetable oils,” Food Chemistry, vol. 151, pp. 47–52, 2014.
1. M. I. Ramli, Z. Zakaria, I. Sahid, T. Y. Ai, and H. Muhamad, “Determination of Herbicide diuron levels in palm oil ma- trices using HPLC-UV,” Sains Malaysiana, vol. 41, pp. 1451– 1459, 2012.
2. T. Tuzimski and T. Rejczak, “Application of HPLC-DAD after SPE/QuEChERS with ZrO2-based sorbent in d-SPE clean-up step for pesticide analysis in edible oils,” Food Chemistry, vol. 190, pp. 71–79, 2016.
3. T. Rejczak and T. Tuzimski, “A review of recent developments and trends in the QuEChERS sample preparation approach,” Open Chemistry, vol. 13, no. 1, pp. 980–1010, 2015.
4. Q. Zhou and Z. Fang, “Graphene-modiﬁed TiO2 nanotube arrays as an adsorbent in micro-solid phase extraction for determination of carbamate pesticides in water samples,” Analytica Chimica Acta, vol. 869, pp. 43–49, 2015.
5. H. Razmi and M. Jabbari, “Development of graphene-carbon nanotube- coated magnetic nanocomposite as an eﬃcient sorbent for HPLC determination of organophosphorus pesti- cides in environmental water samples,” International Journal of Environmental Analytical Chemistry, vol. 95, no. 14, pp. 1353– 1369, 2015.
6. I. Montesinos, A. Sfakianaki, M. Gallego, and C. D. Stalikas, “Graphene-coated cotton ﬁbers as a sorbent for the extraction of multiclass pesticide residues from water and their de- termination by gas chromatography with mass spectrometry,” Journal of Separation Science, vol. 38, no. 5, pp. 836–843, 2015.
7. A. Mehdinia, H. Khani, and S. Mozaﬀari, “Fibers coated with a graphene-polyaniline nanocomposite for the headspace solid-phase microextraction of organochlorine pesticides from seawater samples,” Microchimica Acta, vol. 181, no. 1-2, pp. 89–95, 2014.
8. Z. Shi, Q. Li, D. Xu, Q. Huai, and H. Zhang, “Graphene-based pipette tip solid-phase extraction with ultra high performance

8
Journal of Analytical Methods in Chemistry
liquid chromatography and tandem mass spectrometry for the analysis of carbamate pesticide residues in fruit juice,” Journal of Separation Science, vol. 39, no. 22, pp. 4391–4397, 2016.
1. X. Wu, R. Zhang, X. Liu et al., “Evaluation of graphene for ef- fective cleanup of fruit and vegetable extracts in pesticide residue analysis,” Food Analytical Methods, vol. 8, no. 1, pp. 243–253, 2015.
2. N. Li, J. Chen, and Y. P. Shi, “Magnetic graphene solid-phase extraction for the determination of carbamate pesticides in tomatoes coupled with high performance liquid chroma- tography,” Talanta, vol. 141, pp. 212–219, 2015.
3. W. Guan, C. Li, X. Liu, S. Zhou, and Y. Ma, “Graphene as dispersive solidphase extraction materials for pesticides LC- MS/MS multi-residue analysis in leek, onion and garlic,” Food Additives & Contaminants: Part A, vol. 31, no. 2, pp. 250–261, 2014.
4. M. Zhang, H. Chen, L. Zhu, C. Wang, G. Ma, and X. Liu, “Solid- phase puriﬁcation and extraction for the determination of trace neonicotinoid pesticides in tea infusion,” Journal of Separation Science, vol. 39, no. 5, pp. 910–917, 2016.
5. X. Liu, W. Guan, X. Hao, X. Wu, Y. Ma, and C. Pan, “Pesticide multi-residue analysis in tea using d-SPE sample cleanup with graphene mixed with primary secondary amine and graphitized carbon black prior to LC-MS/MS,” Chromatographia, vol. 77, no. 1-2, pp. 31–37, 2014.
6. R. Sitko, B. Zawisza, and E. Malicka, “Graphene as a new sorbent in analytical chemistry,” TrAC Trends in Analytical Chemistry, vol. 51, pp. 33–43, 2013.
7. M. C. Hurtado-Sa´nchez, R. Romero-Gonza´lez, and
M. I. Rodr´ıguez-Ca´ceres, “Rapid and sensitive on-line solid phase extraction-ultra high performance liquid chromatography– electrospray-tandem mass spectrometry analysis of pesticides in surface waters,” Journal of Chromatography A, vol. 1305, pp. 193– 202, 2013.
1. W. Wang, X. Ma, Q. Wu, C. Wang, X. Zang, and Z. Wang, “The use of graphene-based magnetic nanoparticles as ad- sorbent for the extraction of triazole fungicides from envi- ronmental water,” Journal of Separation Science, vol. 35, no. 17, pp. 2266–2272, 2012.
2. M. Hou, X. Zang, C. Wang, and Z. Wang, “The use of silica- coated magnetic graphene microspheres as the adsorbent for the extraction of pyrethroid pesticides from orange and lettuce samples followed by GC-MS analysis,” Journal of Separation Science, vol. 36, pp. 3242–3248, 2013.
3. X. Wu, H. Zhang, L. Meng, X. Liu, and Y. Ma, “Graphene for
cleanup in trace analysis of pyrethroid insecticides in cucumber and spinach,” Chromatographia, vol. 75, no. 19-20, pp. 1177–
1183, 2012.
EU-Pesticides Database, 2017, http://ec.europa.eu/food/plant/ pesticides/eu-pesticides.

International Journal of
m
o
an

Biochemistry Research International
Hindawi
www.hindawi.com	Volume 2018

Enzyme Research
Hindawi
www.hindawi.com	Volume 2018

Journal of
Nanotechnology
Hindawi
www.hindawi.com	Volume 2018

Journal of
Spectroscopy
Hindawi
www.hindawi.com	Volume 2018

nternational Journal of
Analytical Chemistry
Hindaw
www.hindawi.com	Volume 2018

International Journal of
Electrochemistry
Hindawi
www.hindawi.com	Volume 2018

International Journal of
Spectroscopy
Hindawi
www.hindawi.com	Volume 2018

BioMed
Research International
Hindawi
www.hindawi.com	Volume 2018

Journal of
Chemistry
Hindawi
www.hindawi.com	Volume 2018

Advances in
Tribology
Hindawi
www.hindawi.com	Volume 2018

Journal of
Materials
Hindawi
www.hindawi.com	Volume 2018

Bioinorganic Chemistry and Applications
Hindawi
www.hindawi.com	Volume 2018

International Journal of
Medicinal Chemistry
Hindawi
www.hindawi.com	Volume 2018

Submit your manuscripts at www.hindawi.com

Advances in
Physical Chemistry
Hindawi
www.hindawi.com	Volume 2018

Photoenergy
Hindawi
www.hindawi.com	Volume 2018

Journal of
Applied Chemistry
Hindawi
www.hindawi.com	Volume 2018

The Scientific World Journal
Hindawi
www.hindawi.com	Volume 2018

Journal of
Analytical Methods in Chemistry
Hindawi
www.hindawi.com	Volume 2018
NaJournnaloofmaterials

Hindawi
www.hindawi.com	Volume 2018