Article
# Mutual Diffusion of Model Acceptor/Donor Bilayers under Solvent Vapor Annealing as a Novel Route for Organic Solar Cell Fabrication
Paweł Dąbczyński *, Gabriela Wójtowicz and Jakub Rysz *©
Faculty of Physics Astronomy and Applied Computer Science, Jagiellonian University, ul. Łojasiewicza 11,
30-348 Kraków, Poland; g.wojtowicz@doctoral.uj.edu.pl
* Correspondence: pawel.dabczynski@uj.edu.pl (P.D.); jakub.rysz@uj.edu.pl (J.R.)
©check for
updates
Citation: Dąbczyński, P.; Wójtowicz,
G.; Rysz, J. Mutual Diffusion of
Model Acceptor/Donor Bilayers
under Solvent Vapor Annealing as a
Novel Route for Organic Solar Cell
Fabrication. Energies 2022, 15, 1033.
https://doi.org/10.3390/en15031033
Academic Editor: Adalgisa Sinicropi
Received: 20 December 2021
Accepted: 26 January 2022
Published: 29 January 2022
Publisher's Note: MDPI stays neutral
with regard to jurisdictional claims in
published maps and institutional affil-
iations.
Copyright: © 2022 by the authors.
Licensee MDPI, Basel, Switzerland.
This article is an open access article
distributed under the terms and
conditions of the Creative Commons
Attribution (CC BY) license (https://
creativecommons.org/licenses/by/
4.0/).
Abstract: The fabrication of bulk heterojunction organic solar cells (OSCs) is primarily based on
a phase demixing during solution deposition. This spontaneous process is triggered when, as a
result of a decrease in the solvent concentration, interactions between donor and acceptor molecules
begin to dominate. Herein, we present that interdiffusion of the same molecules is possible when a
bilayers of donors and acceptors are exposed to solvent vapor. Poly(3-hexyl thiophene) (P3HT), and
poly[N-9/-heptadecanyl-2,7-carbazole-alt-5,5-(4/,7;-di-2-thienyl-2/,1/,3/-benzothiadiazole) (PCDTBT)
were used as donors and two types of fullerene derivatives were used as acceptors: phenyl-C61-
butyric acid methyl ester (PC60BM) and phenyl-C71-butyric acid methyl ester (PC70BM), Secondary
ion mass spectrometry depth profiling revealed that the interpenetration of donors and acceptors
induced by solvent vapor annealing was dependent on solvent vapor and component compatibility.
Exposure to chloroform vapor resulted in a complete intermixing of both components. The mutual
mixing increased efficiency of inverted solar cells prepared by solvent vapor annealing of model
donor/acceptor bilayers. These results provide a new means for mixing incompatible components
for the fabrication of organic solar cells.
Keywords: organic solar cells; interdiffusion; solvent vapor annealing
Introduction
Organic solar cells (OSCs) have attracted significant attention as new sources of
renewable energy due to their low cost, light weight and compatibility for large-format
solution deposition production technologies. Phenomenal improvement has taken place
in recent years, and the power conversion efficiency (PCE) of state-of-the-art devices is
comparable with commercially available silicon solar cells [1-4]. This breakthrough could
not have been achieved without new materials [5] and has also been attributed to a better
understanding of the factors that affect OSC fabrication and of the relationship between
microstructure and charge generation [4,6-8].
The basic principles of organic solar cell operation are similar to those for inorganic
devices: excitons created by adsorbed light dissociate and free charge carriers move to
external electrodes. Lower degrees of order of organic semiconductors result in higher
exciton binding energies, lower charge carrier mobility, and higher absorption coefficients.
To promote exciton dissociation, electron acceptors should be placed in the vicinity of
exciton formation regions in donor materials with an uninterrupted path to the external
electrodes. The simplest structure fulfilling such requirements is a donor and acceptor
bilayer sandwiched between electrodes.
This heterojunction concept for organic photovoltaic devices was first investigated
by Tang [9], who showed that a layer of acceptor materials placed between cathode and
donor layers increased the efficiency of low molecular weight organic semiconductor solar
cells. Then, fullerene C60 with its high ionization potential and high electron mobility was
Energies 2022,15,1033. https://doi.org/10.3390/en15031033
https://www.mdpi.com/journal/energies

Energies 2022,15,1033
2 of 14
shown to be an excellent candidate as an acceptor material for highly efficient organic
solar cells [10]. One of the first fullerene devices had fullerene deposited on top of thin
poly(2-methoxy-5-(2;-ethylhexyloxy)-p-phenylene vinylene) film but had no more that
0.04% efficiency. High efficiency light harvesting, exciton dissociation, and charge carrier
transport properties have since been developed for these active layers.
A major breakthrough was achieved with the introduction of a bulk heterojunction [11],
a structure characterized by an interpenetrating network of large interfaces between con-
tinuous donor and acceptor domains. Due to the short lifetimes of excitons in organic
semiconductors, their diffusion length is limited to ca. 10 nm [12,13]. This limits the
characteristic domain size of nanostructured layers. Fortunately, desired structures spon-
taneously form due to phase separation phenomena during the solution coating of thin
multicomponent films on substrates [14].
Studies on model systems, such as poly(3-hexyl thiophene) (P3HT): phenyl-C61-
butyric acid methyl ester (PC60BM), have shown a number of the factors that influence
phase separation allow for the precise control of this spontaneous process to obtain desired
layer morphology [8,15-21]. A lot of work has been done to optimize the coating conditions
of different blends based on solvent composition, constituent blend composition, and
film thickness. Additional studies have been conducted to understand the relationships
between the obtained structures and solar cell properties. Others have also reported on
modifying the properties of these layers. Thermal annealing has been the most often
applied post-treatment method, which typically results in increased P3HT:PC60BM solar
cell efficiency by nearly an order of magnitude [22] due to the enhanced crystallinity of
semiconducting materials. The same effect can be achieved by microwave irradiation [23].
Cell efficiency can also be enhanced by reorganizing the nanostructure of the thin films by
controlling the drying time, i.e., solvent annealing [24] or solvent vapor annealing [25].
Interactions between solutes and solvents are key parameters that affect the demixing
process. Because the number of macromolecule types with the desired electro-optical prop-
erties is limited, the choice of solvent for a selected donor and acceptor mixture is crucial
for obtaining an optimal OSC structure. Theoretical and experimental studies of phase
separation in these ternary systems provide some guidance, but each new donor/acceptor
pair would require optimization. This is because spontaneous demixing occurs rapidly and
is extremely sensitive to slight changes in fabrication conditions. In their seminal paper,
Treat and coworkers [26] revealed thermally induced miscibility in P3HT:PC6oBM and indi-
cated the possibility of using the mixing process to obtain mutually penetrating domains.
Efficient solar cells were fabricated by thermal annealing of P3HT:PC60BM bilayers [27,28].
Further studies on thermally induced intermixing in P3HT/PC60BM system showed com-
plicated interplay between P3HT crystallization and PC60BM interdiffusion [8,21]. The
evolution of the P3HT:PC60BM solar cell performance is shortly summarized in Table 1.
Table 1. Summary of fabrication method and performance of P3HT:PC6qBM solar cells.
Fabrication Method	PCE	Ref.
Thermal annealing of P3HT:PC6qBM blend	4.9%	[22]
Microwave annealing of P3HT:PC6qBM blend	3.6%	[23]
Solvent annealing of P3HT:PC60BM blend	3.64%	[24]
Solvent vapor annealing of P3HT:PC6qBM blend	3.43%	[25]
Solvent vapor annealing + thermal annealing of P3HT:PC6qBM blend	3.7%	[25]
Thermal diffusion of PC60BM/P3HT bilayer	2.41%	[28]
Thermal diffusion of P3HT/PC60BM bilayer (inverted geometry)	1.72%	[28]

The goal of this study is to apply an intermixing method for the fabrication of bulk
heterojunction organic solar cells. For the first time, we show that the interdiffusion of
acceptor/donor bilayers can be induced by solvent vapor annealing and is much slower
than thermal intermixing. The process can be readily controlled by choice of solvent, which
may be more compatible with the first or second component promoting higher mobility.

Energies 2022, 15, 1033
3 of 14
To show this phenomenon can be utilized in fabricating organic solar cells, we prepared
a series of devices with P3HT:PC6oBM and Poly[N-9;-heptadecanyl-2,7-carbazole-alt-5,5-
(4;,7;-di-2-thienyl-2;,1;3-benzothiadiazole) (PCDTBT): phenyl-C71-butyric acid methyl
ester (PC70BM) bilayers exposed to chloroform vapor for different periods. Morphology
and performance comparisons of devices prepared herein were qualitatively consistent
with recently published simulation impact results of vertical composition profiles on OSC
operation.
###### 2. Materials and Methods
Materials. Electronic grade regioregular poly(3-hexyl thiophene) was purchased from
Rieke Metals, Inc. (Lincoln, NE, USA) with a number-average molecular mass Mn = 34 kDa
and a polydispersity index of 2.7. Poly[N-9/-heptadecanyl-2,7-carbazole-fl1f-5,5-(4/,7/-di-2-
thienyl-2;,1;,3;-benzothiadiazole) a number-average molecular mass Mn = 16.2 kDa and
a polydispersity index of 2.15 was purchased from Osilla Ltd. (Sheffield, UK). Phenyl-
C61-butyric acid methyl ester and phenyl-C71-butyric acid methyl ester were obtained
from Solenne BV (Groningen, The Netherlands). Toluene, chloroform, dichloroethane,
tetrahydrofurane, and ZnO ink were purchased from Sigma-Aldrich. All materials and
solvents were used as received.
Interdiffusion of bilayers. Silicon wafers (Si-Mat GmbH, Kaufering, Germany) were
cut into 10 x 10 mm pieces, cleaned by sonification in toluene for 15 min, rinsed with
toluene, and dried with N2 steam. P3HT and PCDTBT were dissolved in chlorobenzene
to form a 15 mg/mL and 5mg/mL solutions, respectively. Before casting, the solutions
were heated at 60 °C overnight inside an argon-filled glovebox. The prepared solution was
filtered through a 0.45-pm syringe filter and spun-cast onto the silicon pieces at 1000 rpm
in the glovebox. Next, the samples were transferred to a vacuum chamber onto which a
layer of PC60BM molecules was thermally evaporated. The layer thickness was monitored
using a quartz microbalance and was adjusted to 50 nm. The bilayer samples were then
transferred back to the glovebox and exposed to different solvent vapors for different time
periods.
Solar cell fabrication and characterization. Solar cells were fabricated using a se-
quential casting routine and thin-film transfer-printing technique [29,30]. Ossila glass
substrates (S211) with patterned ITO electrodes were cleaned by sonication in 2-propanol
for 15 min and dried under N2 flux. Substrates were treated with oxygen plasma, and
zinc oxide nanoparticles were spun cast onto the substrates at 4000 rpm. The prepared
thin films were annealed at 120 ° C for 20 min. P3HT was dissolved in 1,2-dichlorobenzene
to form a 10 mg/mL solution. The solution was heated at 60 °C overnight inside an
argon-filled glovebox and filtered through a 0.45-pm syringe filter prior to spin-casting at
1500 rpm onto prepared ZnO thin films to form an ~30 nm layer. PC60BM was dissolved in
dichloromethane to form an 8 mg/mL solution. Before casting, the solution was heated at
60 °C overnight inside the glovebox. The prepared solution was filtered through a 0.45-pm
syringe filter and spun cast at 1500 rpm onto the prepared ZnO/P3HT thin films to form
an ~90 nm film.
PCDTBT/PC70BM bilayers were prepared by thin-film transfer-printing technique
as described in ref [29]. First PC70BM layer was spun casted from on top of ZnO from
1,2-dichlorobenzene solution (10 mg/mL) filtered through a 0.45 pm syringe filter. PCDTBT
layer was prepared on top of silicon wafer covered with thin film of polystyrene sulfonate
(PSS) by solution casting from 5 mg/mL solution in chlorobenzene. Next flat elastomeric
poly(dimethylsiloxane) (PDMS) stamp was press against the polymer film. After dissolution
of the PSS sacrificial layer in a water bath the stamp with grabbed PDCTBT film was placed
on top of PC70BM layer and gently peeled.
Such prepared bilayers were exposed to chloroform vapor for different durations.
Finally, 100 nm silver electrodes were thermally evaporated to form eight 4-mm2 devices on
each substrate. The solar cells were characterized in an inert atmosphere under white light
illumination from a solar simulator AM1.5 (Newport, Irvine, CA, USA) at 100 mW/cm2;

Energies 2022, 15, 1033
4 of 14
current-voltage characteristics were acquired by a computer-controlled source meter unit,
Keithley 2400 (Keithley Instruments, Solon, OH, USA).
Thin film characterization. The TOF-SIMS experiments were performed on an ION
TOF TOF:SIMS V ins trumcnt (M unster, Germany), equipped with a lCquid metal ion s ource
and a cesium ion rource. Somple depih profile (dSIMS) were obtained in dual beam
mode. Briefly, a 500 eV Cs+ ion beam was used to snuttee-coat a 500 x 500 (rm2 area
and a Bi3+ 30 keV ion beam was used to analyze a 200 x 200 .m2 area concentric to the
sputtered surface.
An Atomic Force Microscope Agilent 5500 instrument was used to investigate the
topography of the free surfaces of the thin films. Set-points and gains were adjusted to
each measurement to obtain clear images without noise. Each topography was investigated
by collecting images at several randomly chosen areas. The images were processed using
Gwyd dion 2.39 toftware.
## 3. Results and Discussion
All experiments described herein include b ilayers of acceptorc on top of joolymer do nor.
Regioregular poly(3-hexyl rhiophene) (P3HT) and poly[I'o-9/-heptadecanyl-2,7-carbazole-
alt-5,5-(4;,7/-di-2-thienyl-2/fi'^-benzothiodiazole) (PCDTBT) were used as model donor
while phenyl-C61-butyric acid mettyl ester (PC60BM) and phenyl-C71-butyric acid methyl
ester (PC70BM) were used as model acceptor. The polymeclayer was spun-coated from
dichlorobenzene solution, whereas tire top layer was prepared by thermal eva.oration [01],
subsequent casting trom dichloroethane [02] or transfer method [l9].The thicknesses ol the
evaporated PC60BM layer were monitored by quartz microbalrnce. The acctntor/donor
bilayers cohere solveirt vapor anneated in a realed container partially filled with selected
soivent. The samples were tlwayr kept separate from liquid solvents. Silicon dicec were
used as substrates -when comparing interdifiusion under different selvent vapors; ITO/ZnO
transparent conductive etectrodes were used for fabricating solar cellr. An experimental
scheme is dep(cted in Figure t.
Figure 1. Experimental scheme of solvent vapor-induced interdiffusion in donor/acceptor. The
bilayer samples were prepared by spin-casting of the first layer followed by: thermal evaporation,
subsequent casting from orthogonal solvent, or transfer with PDMS of the second layer. The samples
were then transferred to a sealed container partially filled with a solvent.
  1. Mutual Diffusion of Acceptor/Donor Bilayers
P3HT thin films covered with PC60BM layers prepared by thermal evaporation were
exposed tto three solvent vapors: dichloroethane (DCE), tetrahydrofurane (THF) and chlo-
roform. Compatibility b etween crganic macromolecules and sclvents were predicfed based
on solubility parameterr 6. The solubil ity parameters of model acceptors and donors are:
6 = 21-22 MPa1-2 2or PC60BM [33], 6 = 12.8-13.1 MPa1/2 for P3HT [34] and 6 = 22.8 MPa1/2
for PCDTBT [35]. The three solvents were selected based on their compatibility with only
one component or with both. Dichloroethane, 6 = 20.2 MPa1/2 [36], is a good solvent
for fullerene derivatives and does not dissolve P3HT nor PCDTBT and was later used
as an orthogonal solvent in sequential casting. Tetrahydrofurane, 6 = 19.4 MPa1/2 [36],
dissolves polythiophene well and PC60BM only slightly. Chloroform, 6 = 19 MPa1/2 [36], is

Energies 2022,15,1033
5 of 14
known to be a good solvent for both PC60BM and P3HT and is often used to fabricate bulk
heterojunction ooganic solar cells.
dSIMS profil es of ehe bilayers prior to and after 1 h exposure to vapors are shown in
Figure 2. The depth profiles monitor variation in composition as a function of sputtering
time. For all silicon substrate samples, C4S- signals (green solid triangles) were usee0 to
determine p3HT content, C2O- oignals (red open circles) for PC60BM content, and Si-
signals (black solid squaresS were usrd to locate interfaces with substeates. The cjuantitative
conversion of sputtering time to intermixed structure depth of P3HT and PCBM is not
straightforward [28]; thus, we precented the profiles as functCons of sputtering time.
Figure 2. SIMS depth profiles of PCgoBM/P3HT bilayers: (a) as-prepared or exposed for 1 h to vapors
of (br THF, (c) DC E, and (d ) chloroform.
"The dSIMS profiles revealed that an initially sharp interface between PC60BM and
polythiophene layers (Figure 2a) slightly broadened when exposed to THF (Figure 2b) or
DCE (Figure 2c( vapors, whereas a single intermixed layer was formed upon exposure
to chloroform vapor (Figure 2d). Sulfur-containing cluster signal characteristics for poly-
thiophene in the top layer increased by an order of magnitude for samples treated with
DCE and THF, whereas for chloroform, this value increased by half that value for pure
P3HT. All samples were prepared under the same conditions, and the initial thicknesses of
both fullerene derivative (44 nm) and polthiophene (55 nm) were the same for all samples.

Energies 2022,15,1033
6 of 14
The bilayer depth profiles indicated large differences in PC60BM and P3HT sputtering
efficiencies. Another factor influencing strongly shape of depth profiles obtained by ion
sputtering methods is the topography of analyzed films [37]. In the profile corresponding to
the as-prepared bilayer sample, the steep increase in Si signal from the substrate was accom-
panied by a rapid signal decrease for polythiophene. In contrast, for samples exposed to
chloroform vapor, the C4S- signal faded long after the silicon signal increased after 1500 s
of sputtering (Figure 2d). This indicated that the initially flat surface of bilayer (Figure 2a)
was roughened when exposed to chloroform vapor. Qualitatively, a similar relationship
between the degree of acceptor and donor interdiffusion and the type of solvent observed
for the PC70BM/PCDTBT layers (not shown).
Detailed analyses of PC60BM/P3HT and PC70BM/PCDTBT bilayer evolution under
solvent vapor annealing in chloroform vapor are presented in Figures 3 and 4. Presented in
Figure 3 dSIMS profiles show progressive mutual penetration of PC60BM and P3HT over
time. While initially sharp, the PC60BM/P3HT interface broadened after 30 min, and the
sulfur signal in the top PC60BM rich layer only slightly increased. The interface flattened
after 45 min and completely diminished after one hour. Detailed analysis of dSIMS profiles
presented in Figure 4 reveals that at the beginning the interface between PC60BM and
PCDTBT moves toward free surface (Figure 4b) and it starts to broaden after 45 min. In
addition increase in the silicon signal is observed already after 1000 s of sputtering for
samples treated for 45 min and longer.
# Sputtering time [s]
Figure 3. SIMS depth profiles of PCggBM/IDHT bilayers: (a) as-prepared or exposed to chloroform
vapor for (b) 30 min, (c) 45 min and (d) 60 min.

Energies 2022,15,1033
7 of 14
Figu re 4. SIMS depth profiles of PCgoBM/PCDTBT bilayers: (a) as-prepared or exposed to chloroform
vapor for (b) 30 min, (c) 45 min and (d) 6(0 min.
A systematic broadening of the substrate interface as determined from silicon signals
indicated increased ftee surface corrugation. This observation is supported by studies on
the evolution of frae surface of bilayers exposed to chloroform vapor. Topographic pictures
presentedin Figure 5a-d show a systematic wrinkling of PC60BM/P3HT bilayer surfaces
with time. Initially, surface undulation amplitude increased (compare Figure 5a,b), followed
by the formfti oo of small holes (Figure 5c), and, aite r (50 min a structure typical of late stage
dewetting phenomenon was observed (Figure 5d). For PQoBM/ZCDTBT (see Figure S1)
high corrugation of the free surface appears after 45 min of chloroform vapor treatment
but no structure typical of late stage dewetting were observed within the experiment.
Quenching of conjugated polymers (donors) fluorescence caused by interactions with
acceptors (PC60MB/PC70BM) allows real-time observation of the intermixing processes
using fluorescent microscopy. Presented in Figure S2 fluorescent micro-graphs show the
initia1 formation of round domains (interssaixed areas) that grow with time to form finally a
strucfure typical of dewetting. We hypothesize that under solvent vapor annealing domains
of saturated donor:acceptor mixtures are formed, aod this process may be followed by
dewetting of excsss os material .

Energies 2022, 15, 1033
8 of 14
Figure 5. Topography of free surfaces of PCgoBM/P3HT bilayer exposed to chloroform vapor for
various periods of time: (a) as-prepared, (b) 30 min, (c) 45 min and (d) 60 min.
  1. Solar Cells
To study the influence of the interdiffusion in acceptor/donor under solvent vapor
annealing on the performance of solar cells, a series of devices on ZnO-covered ITO/glass
electrodes were prepared. Fifst, ZnO ink was cast on top of patterned ITO/glass substrates
and annealed on a hotplate. Next, PCs0BM/P3HT bilayers were prepared by sequential
casting from orthogonal solvents while PCDTBT/PC70BM bilayers were prepared by
transfer method [29,30]. Next bilayers were exposed to chloroform vapor in the same
manner as thf scheme depicted in Figure 1. Finally, metallic electrodes (Ag) were thermally
evaporated through a shadow mask to form eight independent devices on one substrate.
The active area of a single devices was 2 x 2 mm.
SIMS profiles and AFM images obtained lor camples exposed to chloroform vepor for
various time periods showed that the changes in the substrate from silicon to ZnO did not
significantly affect the interdiffusion process (Figures 6 and S3). The C4S- signals (green
solid triangles) were used to determine donof profile, ihe C3O- signals (red open circles)
were used for acceptors, and the 70ZnO- signals (black open squares) were used to locate
the cathode interface. The PC60BM component interpenetrated the polymer layer slightly
during casting, and the interface between fullerene derivative and tire P3HT wae much
broader than samples prepared with thermal evaporation (compare Figures 2a and 3a).
Broadening of the interface between PC70BM and PCDTBT was also observed for samples
prepared by transfer method (see Figure S3).

Energies 2022,15,1033
9 of 14
Figure 6. SIMS profiles and AFM topographic images of PC6oBM/P3HT bilayers prepared on ZnO
and exposed to chloroform vapor for time: ( a) 0 min, (b) 5 min, (c) /0 min and (d) 30 min.
The dSIMS profiles indicated a complete mixing of both phases after 10 min solvent
vapor teeatment. AFM topographic images of samples expesed to solvent vapor longer
than 10 min showed structuses typical of the late stages of the dewetting process. SIMS
composition maps (see Figure S4 in Supporting Materials) indicated the surfaces of lower
domains were reached in sulfur-containing component, whereas the P3HT contents in
higher domains were lower.
Representative current voltage characteristics of solar cells prepared by solvent vapor
annealing of the bilayers are presented in Figure 7. To avoid unpredictable effects of
solvent vapor annealing on PEDOT:PSS, an organic film typically used as a hole-transport
layer, the inverted geometry of solar cells with the ZnO transparent electrode wan chosen.
Initially, the acceptor layer (PC70BM) was in contact with ZnO, the donor PCDTBT with Ag
electrode, and the contact area between donor and acceptor was relatively small. As seen
in Figure 7a), the current-voltage curves shifted down the fourth quarter of the coordinate
aystem with the solvent vapor annealing time as the intermixing of PC70BM and eCDTBT
proceeded. Significantly lower cusrent values obtained for devkes prepared by the layer
transfer method may lesult from the partial degradation of the polymer due to contact
with water.

Energies 2022,15,1033
10 of 14
Figure 7. Representative current-voltage characteristics measured under solar cell illumination
prepared by solvent vapor annealing of (a) PC70BM/PCDTBT and (b) P3HT/PC60BM bilayers for
different time periods.
The initial layer arrangement; of P3HT/PC60BM devices was/ chosen to mimic struc-
Bures classified as unfavorable for charge transport [7] to better show the effects of bulk
heterojunction formation due lo the mutual dfffuslon of acceptor and donor. This was
reflected in the shape of the curuenf-voltage characteristics of the as-prepared devices. Large
slopes of almost linear I-V profiles and low values of the optn circuit voltage Voc were
largely due to energy mismatch levels between the lower layer (P3HT) and the cathode
(ZnO) and the upper layer (PC60BM) and the anode (Ag).
The I-V curves for devices prepared by solvent vapor annealing evolved with treat-
ment time. The open circuit voltage monotonically increased to reach values close to
0.5 V (PC60BM/P3HT) and 0.65 (PC70BMaPiaDTBT) typical for defaces prepared on ZnO;
this was accompanied by increased short circuit current. The maxtoum values of shost
circmt currents and open voltages were observed after 10 min of solverd vapor anneal-
ing for PC60BM/P3HT b.layert and after five minutes for PC70BM/PCDTBT. In case of
the PC60BM/P3HT it corresponds to tht moment when structures typical for late stage
of dewettig begins to form. The faV curves took the shape of a typical solar cell as re-
flected in an increased fill factor, huwever for PC70BM/PCDTBT solar cells decrease in FF
fa observed for longer treatment times. These performance parameters are summarized
for each tolvent vapor treatment time in Figures 8 and S5 (at least eight per data point)
undec AM1.5G solas simulator illumination. Monotonous increases were observed for
efficiency t] (Figuues 8a and S5), short ciccuit curuent IsC (Figures 8b and 515) , open voltage
VOC (Figures 8c and S5) and fill factor FF (Figures 8d and S5) foa device) annealed up to
10 min. Later, nearly all parameters stabilized, but the spreae of their values decreased.
Changes in I-V turves are reflected in the shunt resistances Rsh which for both systems in-
crease with solvent vapor snBealing time /Tables S1 and S2 and Figure S6). However in the
PCDTBT:PC70BM system after initial increase, Rsh drops for annealing times above 1 min.
In this system also series resistance Rs is considerably larger than in the P3HT:PC60BM
tystem which can lee caused by layer transfer, through water, method which can lead to
higher values of Rs in the system.

Energies 2022,15,1033
11 of 14
Figure 8. Performance of solar cells prepared by solvent vapor annealing of PC60BM/P3HT bilayers.
(a) power conversion efficiency; (b) short-current density; (c) open circuit voltage; (d) fill-factor.
An analysis of the data in Figures 8, S5 and S6 and the corresponding SIMS profiles
leads to the conclusion that the cell parameters increased when the donor-rich domains and
acceptor-rich phase s formed large area contacts with the anode and cathode, respectively.
This showed that ahe solvent vapor annualcng of PCr)BMCP3HT and PC70BM/PCDTBT
bilayers leads to the formation of bulk: heterojuoctions after a few minutes. Furthes changes
in film morphology under exposure to solvent vapor did not lead to improved solar cell
efficiency. To exclude a hypothesis that solvent vapor annealing leads to the dewetting
of the acceptor film, P3HT based devices without PCg°BM were prepared and analyzed.
Their efficiency was much lower (0.0017) than that of the devices prepared by sequential
deposition (0.0093). This showed thet a donor-acceptor bulk heterorunction was formed
upon solvent vapor annealing; of the bilayeos.
Our observations were qualitatively consistent with simulation results of the impact
of donor-acceptor vertical composition profiles on OSC performance [7]. The structure
of P3HT/PC60BM devices ap early stages of intermixing ean be classified (according to Bi
eC el. [7]) as unfavorable for charge tronsport. The simulations showed tCat unfavorable
vertical distributions of donors and acceptors leads to a higher recombination of charge
carriers resulting in a lower open circuit voltage Voc consistent with our findings. For the
uniform distribution of donors and acceptors in the active layer, in the devices annealed
for longer durahons, the simulation predicted a higher short circuit cutrent Isc among all
studied structurcc but a smaller VOr than configueations favoring charge transport.
###### 4. Conclusions
We have shown that solvent vapor annealing induced interdiffusion in a model accep-
tor/donor bilayer structure. This phenomenon was used to fabricate an interpenetrating

Energies 2022, 15, 1033
12 of 14
network of acceptor and donor domains for two pairs of model system, P3HT:PC60BM and
PCDTBT:PC70BM. In contrast to phase separation, which has been used to fabricate bulk or-
ganic photovoltaic heterojunction devices, solvent vapor annealing induced interdiffusion
can also be used when there is no common solvent for the donor and acceptor. Observed
intermixing was much slower and allowed for greater control of the final morphology of
the solar cell active layer. This was also slower than thermally induced intermixing and can
be used instead to avoid the high-temperature process of the active layer that is crucial for
devices prepared on flexible surfaces. Further, the ability to select a solvent gives greater
control of the process and potential fine tuning of the final morphology. We demonstrated
that the performance of inverted organic solar cells increased up to the moment when the
intermixed structure of donor and acceptor formed. The general methodology reported
herein provides a new method for fabricating organic solar cells using other recently devel-
oped donor and acceptor (macro)molecules, its advantages may play a positive role in the
commercialization of organic solar cells.
Supplementary Materials: The following supporting information can be downloaded at: https://
www.mdpi.com/article/10.3390/en15031033/s1, Figure S1: Topographic images of PC60BM/PCDTBT
bilayes exposed to chloroform vapor for different time periods: (a) as prepared, 30, 45 and 60 min;
Figure S2. Fluorescence microscopy images of PC60BM/P3HT bilayers prepared on ZnO and exposed
to chloroform vapor for time: (a) 0, (b) 5, (c) 10, and (d) 30 min; Figure S3: SIMS profiles and AFM
topographic images of PC70BM/PCDTBT bilayers prepared on ZnO and exposed to chloroform
vapor for time: (a) 0, (b) 5, (c) 10, and (d) 30 min; Figure S4: SIMS S- images of PC60BM/P3HT
bilayers prepared on ZnO and exposed to chloroform vapor for time: (a) 0, (b) 5, (c) 10, and (d) 30 min;
Figure S5: Performance of solar cells prepared by solvent vapor annealing of PC70BM/PCDTBT
bilayers; Figure S6. Resistances of solar cells prepared by solvent vapor annealing of P3HT:PC60BM
(a) and (b) and PC70BM/PCDTBT (c) and (d) bilayers. Table S1. Performance of solar cells prepared
by solvent vapor annealing of P3HT/PC60BM bilayers; Table S2. Performance of solar cells prepared
by solvent vapor annealing of PC70BM/PCDTBT bilayers.
Author Contributions: The manuscript was written through contributions of all authors. P.D., G.W.,
J.R. have given approval to the final version of the manuscript. All authors have read and agreed to
the published version of the manuscript.
Funding: This project was supported by the National Science Center under Grant No. 2013/11/B/ST5/
04473. The research was performed with equipment purchased thanks to the financial support of
the European Regional Development Fund in the framework of the Polish Innovation Economy
Operational Program (contractno. POIG.02.01.00-12-023/08).
Institutional Review Board Statement: Not applicable.
Informed Consent Statement: Not applicable.
Data Availability Statement: Not applicable.
Acknowledgments: The open-access publication of this article was funded by the Priority Research
Area SciMat under the program “Excellence Initiative-Research University" at the Jagiellonian
University in Krakow.
Conflicts of Interest: The authors declare no conflict of interest. The funders had no role in the design
of the study; in the collection, analyses, or interpretation of data; in the writing of the manuscript, or
in the decision to publish the results.
References
1. Kan, B.; Feng, H.; Yao, H.; Chang, M.; Wan, X.; Li, C.; Hou, J.; Chen, Y. A chlorinated low-bandgap small-molecule acceptor for
   organic solar cells with 14.1% efficiency and low energy loss. Sci. China-Chem. 2018, 61,1307-1313. [CrossRef]
2. Zhang, H.; Yao, H.; Hou, J.; Zhu, J.; Zhang, J.; Li, W.; Yu, R.; Gao, B.; Zhang, S.; Hou, J. Over 14% Efficiency in Organic Solar Cells
   Enabled by Chlorinated Nonfullerene Small-Molecule Acceptors. Adv. Mater. 2018, 30,1800613. [CrossRef] [PubMed]
3. Liu, Q.; Jiang, Y.; Jin, K.; Qin, J.; Xu, J.; Li, W.; Xiong, J.; Liu, J.; Xiao, Z.; Sun, K.; et al. 18% Efficiency organic solar cells. Sci. Bull.
   2020, 65, 272-275. [CrossRef]

Energies 2022, 15, 1033
13 of 14
1. Classen, A.; Chochos, C.; Luer, L.; Gregoriou, V.; Wortmann, J.; Osvet, A.; Forberich, K.; McCulloch, I.; Heumuller, T.; Brabec,
   C. The role of exciton lifetime for charge generation in organic solar cells at negligible energy-level offsets. Nat. Energy 2020, 5,
   711-719. [CrossRef]
2. Xue, R.; Zhang, J.; Li, Y.; Li, Y. Organic Solar Cell Materials toward Commercialization. Small 2018,14,1801793. [CrossRef]
3. Hoefler, S.; Haberfehlner, G.; Rath, T.; Keilbach, A.; Hobisch, M.; Dixon, A.; Pavlica, E.; Bratina, G.; Kothleitner, G.; Hofer, F.; et al.
   Elucidation of Donor:Acceptor Phase Separation in Nonfullerene Organic Solar Cells and Its Implications on Device Performance
   and Charge Carrier Mobility. ACS Appl. Energy Mater. 2019, 2, 7535-7545. [CrossRef]
4. Bi, S.; Ouyang, Z.; Shaik, S.; Li, D. Effect of Donor-Acceptor Vertical Composition Profile on Performance of Organic Bulk
   Heterojunction Solar Cells. Sci. Rep. 2018, 8, 9574. [CrossRef]
5. Westacott, P.; Treat, N.; Martin, J.; Bannock, J.; de Mello, J.; Chabinyc, M.; Sieval, A.; Michels, J.; Stingelin, N. Origin of fullerene-
   induced vitrification of fullerene: Donor polymer photovoltaic blends and its impact on solar cell performance. J. Mater. Chem. A
   2017, 5, 2689-2700. [CrossRef]
6. Tang, C. 2-Layer Organic Photovoltaic Cell. Appl. Phys. Lett. 1986, 48,183-185. [CrossRef]
7. Sariciftci, N.; Braun, D.; Zhang, C.; Srdanov, V.; Heeger, A.; Stucky, G.; Wudl, F. Semiconducting Polymer-Buckminsterfullerene
   Heterojunctions-Diodes, Photodiodes, and Photovoltaic Cells. Appl. Phys. Lett. 1993, 62, 585-587. [CrossRef]
8. Yu, G.; Gao, J.; Hummelen, J.; Wudl, F.; Heeger, A. Polymer Photovoltaic Cells-Enhanced Efficiencies via a Network of Internal
   Donor-Acceptor Heterojunctions. Science 1995, 270,1789-1791. [CrossRef]
9. Halls, J.J.M.; Walsh, C.A.; Greenham, N.C.; Marseglia, E.A.; Friend, R.H.; Moratti, S.C.; Holmes, A.B. Efficient Photodiodes from
   Interpenetrating Polymer Networks. Nature 1995, 376, 498-500. [CrossRef]
10. Halls, J.; Pichler, K.; Friend, R.; Moratti, S.; Holmes, A. Exciton diffusion and dissociation in a poly(p-phenylenevinylene)/C-60
    heterojunction photovoltaic cell. Appl. Phys. Lett. 1996, 68, 3120-3122. [CrossRef]
11. Peet, J.; Heeger, A.; Bazan, G. "Plastic" Solar Cells: Self-Assembly of Bulk Heterojunction Nanomaterials by Spontaneous Phase
    Separation. Acc. Chem. Res. 2009, 42,1700-1708. [CrossRef] [PubMed]
12. Dennler, G.; Scharber, M.; Brabec, C. Polymer-Fullerene Bulk-Heterojunction Solar Cells. Adv. Mater. 2009, 21, 1323-1338.
    [CrossRef]
13. Kroon, R.; Lenes, M.; Hummelen, J.; Blom, P.; De Boer, B. Small bandgap polymers for organic solar cells (polymer material
    development in the last 5 years). Polym. Rev. 2008, 48, 531-582. [CrossRef]
14. Bundgaard, E.; Krebs, F. Low band gap polymers for organic photovoltaics. Sol. Energy Mater. Sol. Cells 2007, 91, 954-985.
    [CrossRef]
15. Thompson, B.; Frechet, J. Organic photovoltaics-Polymer-fullerene composite solar cells. Angew. Chem.-Int. Ed. 2008, 47,58-77.
    [CrossRef]
16. Kippelen, B.; Bredas, J. Organic photovoltaics. Energy Environ. Sci. 2009, 2, 251-261. [CrossRef]
17. Blom, P.; Mihailetchi, V.; Koster, L.; Markov, D. Device physics of polymer: Fullerene bulk heterojunction solar cells. Adv. Mater.
    2007, 19, 1551-1566. [CrossRef]
18. Westacott, P.; Tumbleston, J.; Shoaee, S.; Fearn, S.; Bannock, J.; Gilchrist, J.; Heutz, S.; deMello, J.; Heeney, M.; Ade, H.; et al. On
    the role of intermixed phases in organic photovoltaic blends. Energy Environ. Sci. 2013, 6, 2756-2764. [CrossRef]
19. Reyes-Reyes, M.; Kim, K.; Carroll, D. High-efficiency photovoltaic devices based on annealed poly(3-hexylthiophene) and
    1-(3-methoxycarbonyl)-propyl-1-phenyl-(6,6)C-61 blends. Appl. Phys. Lett. 2005, 87, 083506. [CrossRef]
20. Ko, C.; Lin, Y.; Chen, F. Microwave annealing of polymer photovoltaic devices. Adv. Mater. 2007,19, 3520-3523. [CrossRef]
21. Li, G.; Yao, Y.; Yang, H.; Shrotriya, V.; Yang, G.; Yang, Y. "Solvent annealing" effect in polymer solar cells based on poly(3-
    hexylthiophene) and methanofullerenes. Adv. Funct. Mater. 2007,17,1636-1644. [CrossRef]
22. Zhao, Y.; Xie, Z.; Qu, Y.; Geng, Y.; Wang, L. Solvent-vapor treatment induced performance enhancement of poly(3-hexylthiophene):
    Methanofullerene bulk-heterojunction photovoltaic cells. Appl. Phys. Lett. 2007, 90, 043504. [CrossRef]
23. Treat, N.; Brady, M.; Smith, G.; Toney, M.; Kramer, E.; Hawker, C.; Chabinyc, M. Interdiffusion of PCBM and P3HT Reveals
    Miscibility in a Photovoltaically Active Blend. Adv. Energy Mater. 2011,1, 82-89. [CrossRef]
24. Loiudice, A.; Rizzo, A.; Latini, G.; Nobile, C.; de Giorgi, M.; Gigli, G. Graded vertical phase separation of donor/acceptor species
    for polymer solar cells. Sol. Energy Mater. Sol. Cells 2012,100,147-152. [CrossRef]
25. Chen, D.; Liu, F.; Wang, C.; Nakahara, A.; Russell, T. Bulk Heterojunction Photovoltaic Active Layers via Bilayer Interdiffusion.
    Nano Lett. 2011,11, 2071-2078. [CrossRef]
26. Yim, K.; Zheng, Z.; Liang, Z.; Friend, R.; Huck, W.; Kim, J. Efficient conjugated-polymer optoelectronic devices fabricated by
    thin-film transfer-printing technique. Adv. Funct. Mater. 2008,18,1012-1019. [CrossRef]
27. Abdellah, A.; Falco, A.; Schwarzenberger, U.; Scarpa, G.; Lugli, P. Transfer Printed P3HT/PCBM Photoactive Layers: From
    Material Intermixing to Device Characteristics. ACS Appl. Mater. Interfaces 2016, 8, 2644-2651. [CrossRef]
28. Grzibovskis, R.; Vembris, A. Study of the P3HT/PCBM Interface Using Photoemission Yield Spectroscopy; SPIE: Bellingham, WA, USA,
    2016; Volume 9895.
29. Ayzner, A.; Tassone, C.; Tolbert, S.; Schwartz, B. Reappraising the Need for Bulk Heterojunctions in Polymer-Fullerene Photo-
    voltaics: The Role of Carrier Transport in All-Solution-Processed P3HT/PCBM Bilayer Solar Cells. J. Phys. Chem. C 2009,113,
    20050-20060. [CrossRef]
30. Boucher, D.; Howell, J. Solubility Characteristics of PCBM and C60. J. Phys. Chem. B 2016,120,11556-11566. [CrossRef] [PubMed]

Energies 2022,15,1033
14 of 14
1. Jaczewska, J.; Raptis, I.; Budkowski, A.; Goustouridis, D.; Raczkowska, J.; Sanopoulou, A.; Pamula, E.; Bernasik, A.; Rysz, J.
   Swelling of poly(3-alkylthiophene) films exposed to solvent vapors and humidity: Evaluation of solubility parameters. Synth.
   Met. 2007,157, 726-732. [CrossRef]
2. Biernat, M.; Dabczynski, P.; Biernat, P.; Rysz, J. Phase Separation in PCDTBT:PCBM Blends: From Flory-Huggins Interaction
   Parameters to Ternary Phase Diagrams. Chin. J. Polym. Sci. 2020, 38,1025-1033. [CrossRef]
3. Brandrup, J.; Immergut, E.H.; Grulke, E.A.; Abe, A.; Bloch, D.R. Polymer Handbook; Wiley: New York, NY, USA, 1999.
4. Ziegler, G.; Hutter, H. Correction of topographic artefacts of ToF-SIMS element distributions. Surf. Interface Anal. 2013, 45,
   457-460. [CrossRef]