JSolidStateElectrochem(2014)18:361–368 DOI10.1007/s10008-013-2215-z
The effect of anode surface area on nanoporous oxide formation during anodizing of low purity aluminum (AA1050 alloy)
Leszek Zaraska&Elżbieta Kurowska&
Grzegorz D. Sulka&Ilona Senyk&Marian Jaskula
Received:3June2013/Revised:2August2013/Accepted:5August2013/Publishedonline:17August2013
#The Author(s) 2013. This article is published with open access at Springerlink.com
Abstract Porous anodic alumina layers were obtained by a simpletwo-stepanodizationoflowpurityaluminum(99.5% Al,AA1050alloy)ina0.3Moxalicacidelectrolyteat45V and 20 °C. The effect of anode surface area on structural featuresofnanoporousoxideandprocessofoxideformation was investigated. An ordered structure composed of nano- stripes or nanopores was formed on the Al surface during electrochemicalpolishinginamixtureofperchloricacidand ethanol.Thisnanopatternisthenreplicatedduringtheanodic oxideformation.Itwasfoundthattheporediameter,interpore distance,andporosityincreaseslightlywithincreasingsurface areaofthealuminumsampleexposedtotheanodizingelec- trolyte. On the other hand, a slight decrease in pore density andcellwallthicknesswasobservedwithincreasingsurface areaofthesample.Thedetailedinspectionofcurrentdensity vs. time curves was also performed. The obtained results revealed that the higher surface area of the anode, the local currentdensityminimum,wasreachedfasterduringfirststep ofanodizationandtheincreaseincurrentdensitycorrespond- ing to the pore rearrangement process was observedearlier.
Finally,adensearrayofPdnanowires(∼90nmindiameter) wassynthesizedbysimpleelectrodepositionofmetalinside
the channels of through-hole nanoporous anodic alumina templates with relatively large surface areas (4 cm2).
Introduction
Duringtherecent years, fabricationof 1Dnanostructures suchasnanowiresandnanotubeshasbecomeasubjectofgreat scientificinterestduetoextremelypromisingpropertiesofthese materialsandtheirpotentialapplicationsinmanydifferentareas [1].Aconsiderableattentionhasbeenalsopaidtodevelopmentasimpleandinexpensivemethodofnanofabricationthatcanbeusednot onlyin alaboratory scalebut alsocould havesomepotentialforacommercial-scale implementation[2].Among numerousstrategiesreportedintheliterature,theuseofporousanodic aluminum oxide (AAO) seemstobe oneofthemost popularandeasiest waysforatemplate-assisted synthesisofmetallic,semiconductor,oxide,oreven polymer nanowire ar- rays[3].Nanoporousaluminatemplatescanbesynthesizedby asimpleandcost-effectivetwo-stepanodicoxidationofalumi-numinacidic electrolytes [4]. This process, which doesnotrequireanysophisticatedandexpensive equipment, results information of aluminum oxide layers with aregular,densestructureofhexagonally arrangednanopores. Moreover,struc- turalfeaturesofnanoporous aluminamembranessuchasporediameter,pore-to-poredistance,thicknessof theoxidelayer,etc. can becontrolledbyadjusting anodizing conditions, espe- cially typeofelectrolyteandapplied potentialofelectrolysis[4]. Somedetailed informationon thefabricationofanodicalumina membranesandinfluenceofanodizing conditions on structuralfeaturesandnanoporearrangementofanodicaluminacanbefoundinourprevious works[5–8].
Recently,someattentionhasbeenalsoputontheuseoflowpurity aluminum alloyswith theAlcontentofabout99.5% (e.g., AA1050 alloy) as a starting material for anodization [9–19]. This kind of substrate is very interesting from an economical point of view due to its reasonable price andavailability.Ontheother hand, fabricationofanodicaluminamembranes with a high surface area (up to several squarecentimeters)can beakeyfactorinthetemplate-assisted syn- thesisofnanowiresin alargescale.
KeywordsAnodization.Aluminumalloy.Porousalumina.Pdnanowires
L.Zaraska(*):E.Kurowska:G.D.Sulka:M.Jaskula
Department of Physical Chemistry andElectrochemistry,FacultyofChemistryJagiellonianUniversity,Ingardena3, 30-060Krakow,Poland
e-mail:zaraska@chemia.uj.edu.pl
I. Senyk
DepartmentofElectrochemicalPowerEngineeringandChemistry,KievNationalUniversityofTechnologies&Design,Kiev,Ukraine
ORIGINAL PAPER

362
JSolidStateElectrochem(2014)18:361–368
The main aim of this work was to find out if there is any correlation between the anode surface area and structural featuresandnanoporearrangementofanodicaluminalayers formedbytwo-stepanodizingoflowpurityaluminuminan oxalicacidelectrolyte.Eachstepofnanoporousoxideforma- tion (from Al electropolishing to second anodizing) was discussedindetail.Moreover,wedemonstratedasuccessful fabrication of Pd nanowire arrays using nanoporous anodic aluminamembraneswithrelativelylargesurfaceareas.
chemicaletchingofthebarrierlayerfromthebottomsideof themembranewasperformedbyimmersingthemembranein a 5 wt.% H3PO4solution at 45 °C for 15min.
SynthesisofPdnanowires
PdnanowiresweresynthesizedviaDCgalvanostatic electro-deposition inside the nanochannels of AAO templates. Allexperimentswerecarriedoutin atypical three-electrodecellpowered by a Reference 3000 potentiostat (Gamry Instru-ments).Beforeelectrodeposition,athinAulayerwassputteredonthebottomsideofAAOtemplatestoensuregoodelectriccontact.ThepreparedmembranesservedasworkingelectrodesandPtplateswereusedasboth referenceandcounter elec-trodes. Electrodepositions were performed under a galva-nostatic regimeattheconstant current densityof 2mA/cm2for60min.SolutionofPd(NO3)2(1mg/l)in0.5MHNO3was usedas anelectrolyte. Afterelectrodepositions,samples were rinsedwithwaterandethanolandremainingAAOtemplateswereremovedbychemicaletchingina1MNaOHsolutionfor60min.Finally,thesampleswerecarefully rinsedwithdeion-izedwaterthen withethanolanddried.
Experimental
Synthesisofnanoporousaluminalayers
Nanoporous alumina layers were fabricated by two-stepan-odizationofthe commercially available aluminumfoil(99.5%,typeAA1050).Beforeanodizing,allsampleswere degreased in ethanol and acetone. Then, electrochemical polishing was performed in a mixture of perchloric acid (60 wt.%) and ethanol (1:4 vol.) at 20 V for 1 min. Pt grid wasusedasacathodeduringelectropolishing.Afterthat,the workingsurfaceareasofallsampleswerepreciselydefinedby usinganacid-resistantpaint.Inordertostudytheinfluenceof surfaceareaonstructuralfeaturesofaluminalayers,samples withfourdifferentsurfaceareaswereused(seeTable1).
All samples were anodized under constant potential of 45Vfor1hat20°Cina0.3Moxalicacidsolution.Anodic oxide layers were then removed by chemical etching in a mixtureof6wt.%H3PO4and1.8wt.%H2CrO4at60°Cfor 2 h. As-prepared samples were re-anodized at the same ex- perimental conditions (anodizing potential, electrolyte, and temperature) and the duration of the process was 4 h. After anodizing, samples were rinsed with deionized water and dried. All anodizations were carried out in thermostated double-walledelectrochemicalcells.Pbplatesservedascath- odesandaluminumsamplesasanodes.Thedistancebetween both electrodes was about 2cm.
Characterizationofsamples
Structural features of anodic alumina layers and nanowirearrayswereexaminedwithafield-emission scanning electronmicroscope(FE-SEM/Energy-dispersiveX-ray spectroscopy(EDS), Hitachi S-4700withaNoran System 7).Thecomposi-tionofnanowireswasconfirmedbyEDSanalyses.Character- istic parametersofAAOmembranesweredetermined fromSEMimagesby usingthescanning probeimageprocessor WSxMv.12.0 [20]andImageJ software [21] combined withthe dedicated computational experiment and correspondingexecutable publication [22,23]poweredbythe GridSpace2 platformandCollage Authoring Environment[24].
Results anddiscussion
Fabricationoffree-standingaluminamembraneswitha high-surfacearea
SEMimagesofaluminum surface beforeandafter electro-polishing are shown in Fig.1a,b(low magnification) andFig.1c(high magnification),respectively.It isclearly visiblethat after electropolishing, Al has an almost flat surface(Fig.1b) withsomepits andbumps which couldbeattributedtothelocal allocationofimpurities [17].Ascan beseeninthe high magnification image(Fig.1c), anordered structureiscomposedofnanostripesornanopores formed duringelectro-chemicalpolishing.Theformationofthiskindofnanopatterns,reportedandcharacterizedpreviouslyforhighpurityaluminum [25–33],isprobablyaresultof thepreferential adsorptionofalcohol moleculesonsurface ridges [28,34].The localcross-section profile alongthe lineinFig.1c(Fig.1d)indicatesthat
TheremainingAlsubstratewasremovedinasaturatedsolu- tionofCuSO4containing4wt.%ofHCl.Afterthat,the
Table1 Dimensions of samples used for anodization
Surfacearea (cm2)
Sampletype
Size
AB
C
0.5×0.5 cm
1.0×1.0 cm
1.5×1.5 cm
0.25
1.00
2.25
D
2.0×2.0 cm
4.00

JSolidStateElectrochem(2014)18:361–368
363
Fig.1SEMimagesofaluminum surface before(a)and after electropolishing(b,c)together withanintensityprofilealongthe blue line in c (d). Thesurfaceareaofthesamplewas0.25cm2
thewavelengthofthecreated stripe patternisbetween60and70 nm. This finding is in perfect agreement with resultsobtainedbyKongetal.[28].Besidesthetypicalstripepattern,acellular pattercanbefoundinsome areasofelectropolishedaluminum,especiallynear pitsordislocations(seeFig.1c).Somerecent works [28,34]claimthat the kindofnanostruc-tures obtained during electropolishing dependsnotonlyonapplied voltagebutalsoondurationoftheprocess.Moreover,the size ofnanosized patterns formedontheAlsurfaceduring
electropolishing increaseswith theapplied potential[33].Thedetailed investigationon thisphenomenonisnowinprogress.TheSEMimageofaluminumoxidelayerafterfirstanod-ization is shown in Fig.2b. Theirregular,nanoporousstruc-turewithrandomlydistributedporesof20–30nmindiametercanbeeasilyrecognized.AbriefcomparisonofimagesshowninFig.2a,bindicatesthatthenanopatterncreatedonthealuminumsurfacebyelectropolishingisthenreplicateddur-ingtheanodicoxideformation.Toconfirmthis,ananopore/
Fig.2SEMimagesofAlsurface after electropolishing (a), aluminumoxideafterthefirststep of anodizing (b), metalsurfaceafter oxide removal(c),and porousaluminaaftersecondstep ofanodization(d).The surface areaofthesampleswas2.25cm2. Anodization was carried outin
0.3 M oxalic acid at 20 °C under 45 V. The duration of first and second anodizing step was 1 and 4 h, respectively

364
JSolidStateElectrochem(2014)18:361–368
nanostripespacingwascalculatedforallsamplesbeforeand after first anodizing (Fig.3). The results prove that themor-phologyofinitialnanoporousoxideisstronglydeterminedby the morphology of aluminum substrate used as a starting material. In our experiments, after the first anodizing step,weobserved initial growthofpores along thelinearnanopatternformedduringelectropolishing.Belowthislinear pore structure, the hexagonally arranged pores are visible. This suggest that, according to the mechanism proposed by Jessensky et al. [35], re-arrangement of pores occurs with anodizingtimeandrepulsiveforcesbetweentheneighboring poresplayacrucialroleintheporousoxidegrowth.
According to the point defect model (well describing the pore initiation during anodization) [36,37] and generally accepted the field-assisted dissolution model, the growth of porousoxideoccursatthemetal/oxideinterfaceorveryclose tothisinterface[26,38,39].Duringtheporerearrangement process(seebelow),thesizeofporesformednearthemetal surface increases, while the pore density decreases, mainly due to the merging of adjacent pores. In consequence, the oxide structure found underneath exhibits much larger pore diametersandinterporedistancesthanthatinitiallyformedat the beginning of anodization. The thickness of outerlayer,withthestructuredeterminedbythenanopatternformeddur-ingelectropolishing,isthenreducedduringanodizingduetoa field-assisted dissolution of Al2O3at the oxide/electrolyte interfaceoccurringintheacidicelectrolyte.Thisfactiswell illustratedinFig.3bwherebeneaththesurface,afragmentof aninneroxidelayerwithmuchlargerporesandporespacing unveiled during anodizing can be easilyseen.
A typical morphology of aluminum surface after oxide removal is shown in Fig.2c. As can be seen, a dense array of hexagonally arranged concaves is formed during thefirst anodizing step. These shallow concaves serve as initiation pointsfortheporeformationduringsecondanodizing.An
averagespacingbetweenthesenanoholeswascalculatedfor all anodized samples. It was found that the averagedistance between concaves, which depends mainly on the applied potential [4], equals to115±10nm for 45 V independently of surface area of the sample. The potential of 45 V was chosen as a potential at which the best hexagonal nanopore arrangement is observed[4].
The SEM image of nanoporous oxide after the second anodization is shown in Fig.2d. As can be easily seen,pore diameterandinterporedistancearelargerthanthoseobserved just after the first anodizing step; that can be proved by comparisonofvaluesfromFigs.3aand4a.Moreover,amuch betterhexagonalarrangementisobservedfortheoxidestruc- tureafterthesecondanodizingstep.Thisisobviouslyadirect resultofthefactthatnanoconcavesformedontheAlsurface duringthefirstanodizationinitiateporenucleationduringthe secondanodization.Fortheanodizedsampleswithdifferent surface areas, all structural features of as-obtained porous anodic alumina layers were determined directly from SEM images.Firstly,allnanoporeswereidentifiedbyImageJsoft- ware [21] and such parameters as area and center of mass coordinates were determined for each pore. These raw data were next preceded by the dedicated executablepublication [22,23] in order to obtain the average pore diameter (Dp), interpore distance (Dc), pore density(ρ),porosity(σ),and degree of poreorder.The effect of anode surface area on structuralfeaturesofanodicaluminaisshowninFig.4.The results indicate that pore diameter increases withincreasing surfaceareaofthealuminumsampleexposedtotheanodizing electrolyte.Moreover,a slight increase in interporedistance can be observed. As a consequence, thinner cell walls are observedforsampleswithlargesurfaceareas(seeFig.4a).
Duetothelackofregular,hexagonalarrangementofpores, poredensity,defined as number of pores per 1 cm2surface area,andporosity,definedasaratioofthesurfacearea
Fig. 3 A comparison between pore to pore distance afterelectropolishingand after the first step of anodizing(a).SEM image ofnanoporousoxide formed at the sample with a surface area of 2.25 cm2after the first anodizing step(b)

JSolidStateElectrochem(2014)18:361–368
365
Fig.4Valuesofinterporedistance,porediameter,andwallthickness(a),porosityandporedensity(b)forsampleswithdifferentsurfaceareasafterthe second step ofanodization
occupied by pores to the whole surface area of the sample, were calculated directly from SEM images. The results are showninFig.4b.Withincreasingsurfaceareaofthesample,a slight decrease in pore density was observed;however,this dependence is not statistically significant. It is an obvious consequence of increasing pore spacing. On the other hand, structureswithhigherporositieswereobtainedwhensamples with large surface areas were used foranodization.
A degree of nanopore order was also investigated. Thenanoporearrangementforsampleswiththelowestandhighestsurface areaswasvisualizedbyapplyingacolor coding algo- rithmproposedbyHillebrandetal.[40].Thisapproachisbasedonassigningcolorstoporeswhichdifferintherelativeangularorientationoftheir basicpattern.As aresult,anytransitionbetween domainsisindicatedas achangein thecolorsofindividual pores. Defect maps, knownasDelaunaytriangula-tions,wereconstructedonthebasisofporecenterscoordinatesbyusing dedicated executable paper poweredbyGridSpace2
andmarkedinblack.Ascanbeseen, nanostructureswithaquite poor hexagonal arrangementareobtainedwhenalowpurity aluminumisusedas astarting materialand thisisin agreementwith ourprevious findings [17].Thepercentageofdefects, definedas aratio betweenthenumberofdefective poresand thenumberofallporesontheanalyzed surface was foundtobeabout40%forallstudiedsamplesindependentlyoftheanode surfacearea.
Typical dependences between current density and timerecorded duringanodizationsareshowninFig.6. Inallcases,arapiddecreaseincurrentdensityisobservedduringtheinitialperiodofanodizationas aresultofthe compactandhigh-resistant oxide layer growthon theAlsurface.Afterreachingthelocalminimum,anincreaseincurrentdensity,beingadirectconsequenceoftransformationofthecontinuousoxidelayerinto porouslayer,is observed. Then, the curve shows thedesired value whichistheevidenceoftheporerearrangementprocess.Finally,thecurrent density doesnotchangesignifi-cantlywith time andasteady-state formationofporous oxideoccurs. As can be seen in Fig.6a, there is asignificant
Virtual Laboratory [22,23]
(Fig.5). The pores not sixfold
coordinatedbyneighboring poreswererecognizedasdefects
Fig.5 Mapsofporesafterapplyingthecolorcodingalgorithmforsampleswithsurfaceareaof0.25cm2(a)and4cm2(b)afterthesecondstepof anodization

366
JSolidStateElectrochem(2014)18:361–368
Fig. 6
Currentdensityvs.timecurvesrecordedduringtheAA1050alloy
surface areas (b), curves recorded during the second anodization of samples with different surface areas (c)
anodization.Comparisonbetweenthefirstandsecondanodizingstep(a),
curves recorded during the first anodization of samples with different
differenceinthecurrent densityvs. timedependenceforfirstandsecond anodizing steps. Whentheanodic alumina film grows, the current density minimum observed duringthefirstanodizationisdeeperthan inthe case when the aluminumsurfaceispretexturedandusedforthesecondanodization.Thiscanbeattributedtothefactthatatthebottomofeachconcave,thelowest resistanceandhighest electric fieldareobserved.Therefore, the pore nucleation occurs much easier on thepretextured surface.Inconsequence,thelower rateofbarrieroxidegrowthandthemorerapidincreaseincurrentdensityare
observed.Itshouldbementioned thatthecurrent–time curve recordedfor theAA1050 foilisverysimilartothose obtainedbyLietal.[26]andWangetal.[41]forhigh-purityaluminum.Forinitial10 minoffirst anodizations, currentvs. timedepen-denceswererecordedfor allsampleswithdifferentsurfaceareas.As canbeseeninFig.6b, thehigher surface areaoftheanode,thelocalcurrentdensityminimumisreachedfasterandthe increase in current density corresponding to the porerearrangementprocessisobservedearlier.Thiscouldbeattrib- utedtothefact thatthehigher surfaceareaoftheanodeisthe
Fig.7FE-SEMimageofPdnanowires(a)togetherwiththeirEDXspectrum(b).TheDCelectrochemicaldepositionwasperformedat2mAcm−2for 60min

JSolidStateElectrochem(2014)18:361–368
367
moredefects,likebumps,holesetc.,onthemetalsurfaceexists.Obviously,the densityofdefects, i.e., numberofdefectspersurfaceareaunit,isexpectedtobethesamebutforlargesurface areas, mechanical integrityof thebarrier oxide layerismore difficulttobemaintainedandbreakingofthecontinuousdi-electric layercanoccurearlier.Ontheother hand,anoppositetrendwasfound when currentvs. timecurves recordedduringthesecond anodizing step were compared.Ascan beseeninFig.6c, theminimumincurrent densityisreached fasterforsampleswithalowsurface area.Moreover,not only thetime after whichthecurrent density minimumisobservedbutalsothedepthofthisminimumincreasewithincreasingsurfaceareaoftheanode.Itwouldindicatethatthesamplewiththesmallestsurface areawaspretextured moreeffectivelyduring thefirststepofanodization.
TheAAOtemplateswithasurfaceareaof4cm2wereusedastemplatesforthefabricationofdensearrayofPdnanowires.Asitwasmentionedabove,justafterthesecondanodizingstep,theremaining aluminumwaschemically removedbyimmer-sion in the solution of HCl+CuSO4. Then, the continuousoxide layeratthepore bottomswasetchedin aphosphoricacid solution (for details see“Experimental”section) andthrough-holeAAOtemplateswereobtained. After sputteringofthethinAulayeronAAO,Pdwaselectrochemicallydepos-itedinsidetheporesofaluminatemplate.AtypicalSEMimageofthePdnanowire array releasedfrom thealumina template togetherwith the EDSanalysisisshowninFig.7. Thedense arrayofcontinuous, homogenousinshape,and parallelPd nanowireswith anaverage diameterofabout90 nmcanbe easily recognized.TherecordedEDSspectrum confirmed thecomposition of nanowires; however, the Au and C peaksresulting fromthethin layer sputtered beforeelectrodepositionon the bottom side of the alumina template and from theconductive carbon pasteusedduringSEMimagingarealso noticeable.ThiskindofPdelectrodescanbeaverypromisingmaterialformany potential applications, e.g., sensors [42,43]and catalysis [44]; however, some problems with uniformfillingofnanoporeswithmetal still shouldbesolved.
comparisonofmorphologyofnanoporousoxidelayersformedafter the second step of anodizing indicated that the porediameter,interporedistance,andporosityincreaseslightlywithincreasingsurfaceareaofthealuminumsampleexposedtothe anodizing electrolyte.Ontheother hand,withincreasing sur- faceareaofthesample,aslight decreaseinporedensityandcell wall thicknesswasobserved. Current–time behavior wasalsoinvestigatedforallanodizedsamples.Itwasfoundthatthe higher surfacearea of theanode duringthefirststepofanod- ization,thelocalcurrentdensityminimumisreachedfasterandthe increase in current density corresponding to the porerearrangement processisobservedearlier.Anoppositetrendwasfound when currentvs. timecurves recorded during the secondanodizingstepwerecompared.Finally,wedemonstrat-
ed asuccessful fabricationofPdnanowire arrays (∼90nmin diameter) using nanoporous anodic alumina membranes with
relatively large surface areas (4 cm2).
Acknowledgments The research was partially carried out with the equipmentpurchasedthanks to the financial support of the European RegionalDevelopmentFundintheframeworkofthePolishInnovation EconomyOperationalProgram(contractno.POIG.02.01.00-12-023/08).This work was made possible with assistance of the PL-Grid project,contract number: POIG.02.03.00-00-007/08-00, website:www.plgrid.pl.Theprojectisco-fundedbytheEuropeanRegionalDevelopmentFundas part of the Innovative Economy program. The SEM imaging was performed in theLaboratoryof Field Emission Scanning Electron Mi- croscopy and Microanalysis at the Institute of Geological Sciences,Jagiellonian University,Poland.
OpenAccessThis article is distributed under the terms of theCreativeCommonsAttributionLicensewhichpermitsanyuse,distribution,and reproduction in any medium, provided the original author(s) and the source arecredited.
References
1. ZhaiT,YaoJ(eds)(2013)One-dimensionalnanostructures:princi-ples and applications.Wiley,Hoboken,NJ
2. ChenS(ed)(2010)Nanomanufacturing.AmericanScientific,NewYork
3. Sulka GD, Zaraska L, Stępniowski WJ(2011)In. Nalwa HS(Ed).Encyclopediaof nanoscience andnanotechnology,vol11,2nd ed.American Scientific: California. pp261–349
4. Sulka GD (2008) In: Eftekhari A (ed) Nanostructured materialsinelectrochemistry.Wiley,Weinheim,pp1–116
5. SulkaGD,StroobantsS,MoshchalkovV,BorghsG,CelisJP(2002) J Electrochem Soc149:D97–D103
6. SulkaGD,ParkołaKG(2006)ThinSolidFilms515:338–345
7. Zaraska L, Sulka GD, Jaskuła M(2011)J Solid StateElectrochem15:2427–2436
8. ZaraskaL,StępniowskiWJ,CiepielaE,SulkaGD(2013)ThinSolid
Films 534:155–161
1. AertsT,DimogerontakisT,DeGraeveI,FransaerJ,TercynH(2007) Surf CoatTechnol201:7310–7317
2. Montero-MorenoJM,SarretM,MüllerC(2007)SurfCoatTechnol201:6352–6357
3. Montero-MorenoJM,SarretM,MüllerC(2007)JElectrochemSoc 154:C169–C174
4. YuC,HuC,BaiA,YangY(2007)SurfCoatTechnol201:7259–7265
Conclusions
The effect of anode surface area on the nanoporous oxideformationduringanodic oxidationoflow-purityaluminum was studied in detail. It was confirmed that an orderednanostripeornanopore structureisformedontheAlsurfaceduring electrochemical polishingand thewavelengthofthe created stripe patternwasfoundtobebetween60and70nm.Itwasrevealed thatthenanopattern createdonthealuminum surfacebyelectropolishingisthenreplicatedduringtheanodicoxide formation. Duringthe porerearrangement process, thesizeofporesformednearthemetalsurfaceincreases,whilethe poredensitydecreasesduetothemergingofadjacentpores.A

368
JSolidStateElectrochem(2014)18:361–368
1. BaiA,HuC,YangY,LinC(2008)ElectrochimActa53:2258–2264
2. Fernández-Romero L, Montero-Moreno JM, Pellicer E, PeiróF,Cornet A, Morante JR, Sarret M, Müller C (2008) Mater Chem Phys111:542–547
3. ShihT,WeiP,Huang Y (2008) Surf Coat Technol 202:3298–3305
4. Montero-MorenoJM, Belenguer M, Sarret M, Müller CM (2009)Electrochim Acta54:2529–2535
5. Zaraska L, Sulka GD, Szeremeta J, Jaskuła M (2010)Electrochim
Acta 55:4377–4386
1. ZaraskaL,SulkaGD,JaskułaM(2010) SurfCoatTechnol205:2432–2437
2. Michalska-Domańska M, Norek M, Stępniowski WJ,Budner B
(2013) Electrochim Acta 105:424–432
1. HorcasI,FernándezR,Gómez-RodríguezJM,ColcheroJ,Gómez-HerreroJ,BaroAM(2007)RevSciInstrum78(013705):1–8
2. ImageJ.NationalInstituteofMentalHealth.Bethesda,MD,USA.http://rsb.info.nih.gov/ij
3. Ciepiela E, Zaraska L, Sulka GD (2012) Lect Notes ComputSci7136:240–251
4. CiepielaE,ZaraskaL,Sulka GD.Implementationofalgorithmsofquantitative analysisofthe grainmorphologyinself-assembledhexag-onallattices accordingtoHillebrand method. ExecutablepublicationpoweredbyGridSpace2platform,hostedinAcademicComputerCentreCYFRONETAGH,http://gs2.cyfronet.pl/epapers/hillebrand-grains/
5. NowakowskiP,Ciepiela E, Harężlak D, Kocot J, Kasztelnik M, BartyńskiT,Meizner J, Dyk G, Malawski M(2011)Proc ComputSci 4:608–617
6. Shimizu K, Kobayashi K, SkeldonP,Thompson GE,WoodGC(1997)Corros Sci39:701–718
7. LiF,ZhangL,MetzgerRM(1998)ChemMater10:2470–2480
1. Guo DZ, Hou SM, ShenZY,ZhaoZY,Liu WM, Xue ZQ (2002)Chin Phys Lett19:385–388
2. KongLB,HuangY,GuoY,LiHL(2005)MaterLett59:1656–1659
3. GhorbaniM,NasirpouriF,IrajizadA,SaediA(2006)MaterDesign 27:983–988
4. Rauf A, Mehmood M, Asim Rasheed M, Aslam M (2009) J Solid State Electrochem13:321–332
5. Sarkar J, Gopal Khan G, Basumallick A (2009) Nanotechnology 20(095604):1–7
6. Huang K, Huang SM, Pu L, ShiY,WuZM, Ji L, Kang JY (2010)Nanoscale Res Lett5:1977–1981
7. WangN, Zhang WD, XuJP,Ma B, Zaho ZZ, JinQY,Bunte E,HupkesJ,BochemHP(2010)ChinPhysLett27(066801):1–4
8. YuzhakovVV,ChangSC,MillerAE(1997)PhysRevB56:12608–12624
9. JessenskyO,MüllerF,GöseleU(1998)ApplPhysLett72:1173–1175
10. Macdonald DD(2011)Electrochim Acta56:1761–1772
11. Macdonald DD(1992)J Electrochem Soc139:3434–3449
12. Thompson GE (1997) Thin Solid Films297:192–201
13. ZhuXF,SongY,LiuL,WangCY,ZhengJ,JiaHB,WangXL(2009)Nanotechnology20(475303):1–7
14. HillebrandR,MullerF,SchwirnK,LeeW,SteinhartM(2008)ACSNano2:913–920
15. WangN,ZhangW,XuJ,MaB,ZhangZ,JinQ,BunteE,HüpkesJ,BochemHP(2010)JSolidStateElectrochem14:1377–1382
16. ImY,Lee C,VasquezRP,Bangar MA, MyungNV,Menke EJ,Penner RM,YunM (2006) Small2:356–358
17. WenD, Guo S, Dong S,WangE (2010) Biosens Bioelectron26:1056–1061
18. Sun Z, ChengF,Dai X (2009) J Autom Methods Manag Chem 496281/1–5