www.nature.com/scientificreports
OPEN
Structural, electrical, and magnetic
study of La‑, Eu‑, and Er‑ doped bismuth ferrite nanomaterials obtained by solution combustion synthesis
Angelika Wrzesińska1, Alexander Khort2,3, Marcin Witkowski4, Jacek Szczytko4,
Jacek Ryl5, Jacek Gurgul6, Dmitry S. Kharitonov6,7, Kazimierz Łątka8, Tadeusz Szumiata9 & Aleksandra Wypych‑Puszkarz1
In this work, the multiferroic bismuth ferrite materials Bi0.9RE0.1FeO3 doped by rare‑earth (RE = La,
Eu, and Er) elements were obtained by the solution combustion synthesis. Structure, electrical, and magnetic properties of prepared samples were investigated by X‑ray photoelectron spectroscopy, Mössbauer spectroscopy, electrical hysteresis measurement, broadband dielectric spectroscopy, and SQUID magnetometry. All obtained nanomaterials are characterized by spontaneous electrical polarization, which confirmed their ferroelectric properties. Investigation of magnetic properties
at 300.0 K and 2.0 K showed that all investigated Bi0.9RE0.1FeO3 ferrites possess significantly higher magnetization in comparison to bismuth ferrites obtained by different methods. The highest saturation magnetisation of 5.161 emu/g at 300.0 K was observed for the BLaFO sample, while at
2.0 K it was 12.07 emu/g for the BErFO sample. Several possible reasons for these phenomena were proposed and discussed.
Bismuth ferrite BiFeO3 is a multiferroic that belongs to the group of materials with a perovskite-type ABO3 crystal structure. Such crystal structure is formed through a network of corner-linked oxygen octahedra. The unit cell of BiFeO3 has rhombohedral (R3c) symmetry with lattice parameters: a = 5.58 Å and c = 13.90 Å1. The larger cation (Bi3+) occupies the A site in the corner position of the unit cell and mostly defines BiFeO3 ferromagnetic polarisation. Smaller cations (Fe3+) occupy the B site in the face-centered position and are related to the mag- netic properties of BiFeO3, while oxygen ions are located in the body-centered positions2. Due to the ionic sizes of bismuth and oxygen, the BiFeO3 structure does not perfectly match the ideal cubic unit cell. Therefore, the oxygen octahedra are tightened in order to fit into the reduced cell. This leads to the rotation of oxygen octahedra in BiFeO3 around the polar [111] axis by the angle of 11–14° and directly affects the value of the Fe–O–Fe bond angle3. The magnetic exchange interaction, which is related to the bond angle, and the orbital overlap between iron and oxygen can significantly influence the magnetic ordering temperature and the conductivity of the BiFeO3 phase. These structural features lead to simultaneously ferroelectric (Curie temperature TC = 1103 K) and magnetic (Néel temperature TN = 643 K) behaviors of BiFeO3 at ambient temperature.
Other important features of the BiFeO3 phase are related to its magnetic structure. It adopts a G-type anti- ferromagnetic ordering, i.e. each Fe3+ spin is surrounded by six antiparallel spins of the closest Fe neighbours4. However, these spins are not perfectly antiparallel and exhibit weak canting moments due to the local magneto- electric coupling to the polarization. The existence of canting creates a long-range arrangement of a spin-cycloid
1Lodz University of Technology, Zeromskiego 116, 90-924 Lodz, Poland. 2KTH Royal Institute of Technology, Stockholm, Sweden. 3National University of Science and Technology “MISIS”, Moscow, Russia. 4University of Warsaw, Pasteura 1, 02-093 Warsaw, Poland. 5Gdańsk University of Technology, 11/12 Narutowicza st, 80-233 Gdańsk, Poland. 6Jerzy Haber Institute of Catalysis and Surface Chemistry, Polish Academy of Sciences, Niezapominajek 8, 30239 Kraków, Poland. 7Research and Development Center of Technology for Industry, Ludwika Warynskiego 3A, 00645 Warsaw, Poland. 8Marian Smoluchowski Institute of Physics, Jagiellonian University, Łojasiewicza 11, 30-348 Kraków, Poland. 9Kazimierz Pulaski University of Technology and Humanities in Radom, Stasieckiego Str. 54, 26-600 Radom, Poland. email: angelika.wrzesinska@edu.p.lodz.pl; khort@kth.se
Scientific Reports |
(2021) 11:22746
| https://doi.org/10.1038/s41598-021-01983-z
1

www.nature.com/scientificreports/
of the antiferromagnetically ordered sublattices with a period of ca. 62–64 nm and the propagation vector along the [110] direction1. Due to the presence of spin cycloid structure, a larger part of the net magnetic moment is cancelled and the magnetoelectric coupling is inhibited. Nevertheless, canting of the spin structure in BiFeO3 leads to antisymmetric spin exchange (Dzyaloshinskii–Moriya interaction), resulting in a presence of relatively small ferromagnetic moment5–7. A slightly higher magnetic moment can be observed for BiFeO3 nanoparticles, for which there is a considerable contribution of uncompensated ferromagnetic spin alignment at the surface8,9. As a result of their unique properties, for the past 20 years BiFeO3 and BiFeO3-based materials have been widely explored to be used in a broad range of applications in advanced electronics, such as spintronics and information storage (ferroelectric random access memory (FeRAM)10, and in magnetic random access mem- ory (MRAM)11), photovoltaic12, and sensor devices13, hyperthermia treatment14, photocatalysis2,15–17, and as supercapacitors18,19. Unluckily, a number of disadvantages hinder the widespread use of BiFeO3-based nano- materials. Among them are low resistivity, resulting from high leakage current inducing large dielectric loss, small remnant polarization, and weak ferroelectric loop at room temperature. For the above-mentioned effects, the oxygen vacancies and secondary phases that nucleate at grain boundaries are responsible. They are difficult to avoid during synthesis and they require careful attention to processing parameters20. Moreover, the volatile nature of Bi3+ during synthesis causes reduction of Fe3+ to Fe2+ and formation of anion and cation vacancies. Applicability of this material is also limited due to the presence of complex incommensurate cycloid magnetic structure, which is responsible for weak magnetoelectric coupling21. One of the most efficient ways to improve magnetic and ferroelectric properties is ion substitution that induces lattice distortions and decreases particle size, as well as suppresses cycloid spin structure. A broad range of elements was tested as dopants in the A-site or B-site positions in order to influence the internal structure of BiFeO3 and suppress the formation of the second- ary phase during synthesis. The rare-earth metals have repeatedly confirmed their positive contribution to the properties of doped BiFeO3. Reddy et al.2 observed the improvement in photocatalytic efficiency, higher specific capacitance values with increasing La doping (LaxBi1-xFeO3, x = 0.01–0.10) and reaching the highest values of coercivity (315 Oe), and saturation magnetisation (0.83301 emu/g) at 10% of La doping. Hong et al.22 reported that 5% doping of trivalent ions Sm3+, Gd3+, and Y3+ in BiFeO3 improved ferromagnetism due to modulation of spiral spatial structure. Golda et al.23 observed enhancement of dielectric, ferromagnetic and electrochemical
properties of Sm-doped BiFeO3 (Bi1-xSmxFeO3; x = 0.05 and x = 0.1).
Up to now different synthesis methods were reported for successful obtaining of BiFeO3-based materials: RF magnetron sputtering24, polymer solution method25, solution combustion synthesis (SCS)26. The SCS method is based on exploiting a highly exothermic combustion redox reaction between metal nitrates (oxidizer) and organic fuel (reducer), mixed in the solution. The SCS deserves special attention as it is considered to be time and energy-saving and easy to scale up27–29. Besides, this method has been successfully used for the synthesis of a broad variety of materials, including metals30,31, graphene32, simple and complex oxides including BiFeO333–35, so far only a few works have described the application of the SCS for rare-earth-doped BiFeO3 preparation36.
The present study evaluates the effect of a high-load (10%) La, Er, and Eu doping on the crystallographic structure, magnetic and electrical properties of co-doped BiFeO3 nanoparticles obtained by the SCS method.
Materials and methods
Synthesis procedure. The detailed procedure for the synthesis of examined materials is described in our previous article36. Herein we report only the general description of the main steps.
All materials were prepared using the microwave-assisted solution combustion synthesis (SCS) as follows. Bismuth(III)-nitrate pentahydrate (Bi(NO3)3∙5H2O), iron(III)-nitrate nonahydrate (Fe(NO3)3∙9H2O) and one of the rare-earth metal nitrates (La(NO3)3∙6H2O, Eu(NO3)3∙6H2O or Er(NO3)3∙6H2O) were dissolved in an acidic aqueous solution in such ratios to form the final material with stoichiometric formula Bi0.9RE0.1FeO3. In the text of the paper, they are further abbreviated as BFO (BiFeO3), BLaFO (Bi0.9La0.1FeO3), BEuFO (Bi0.9Eu0.1FeO3), and BErFO (Bi0.9Er0.1FeO3). The citric acid (CA) was used as a fuel (reducer). The parameter φ, which is the fuel-to- oxidizer molar ratio, for all experiments was kept constant and equal to 1.25. The obtained solution containing all precursors was rapidly dried in a microwave oven (800 W, 2.450 GHz) until a gel and then highly porous foam had formed. The foam was ignited and burned in a preheated muffle furnace at 573 K in air, leading to the formation of a fluffy brown powder. The obtained powder was hand-milled in an agate mortar and annealed in air at 923 K for 30 min with rapid heating and cooling by means of quenching, after which the resulting powder
was hand-milled again. It is assumed that in the systems under study Bi3+ is substituted by close in size La3+ and
3+
3+
3+
3+
smaller Eu and Er ions (rBi	= 1.03 Å, rLa	= 1.03 Å, rEu	= 0.95 Å, and rEr	= 0.89 Å, respectively) .
3+
3+
37
ion
ion
ion
ion
Characterization. The X-Ray Photoelectron Spectroscopy (XPS) measurements were carried out in a high-resolution mode, with a pass energy of 20 eV. The studies were performed on an Escalab 250Xi from ThermoFisher Scientific. The spectroscope utilizes monochromatic Al Kα X-ray source with a spot diameter of 650 µm. The charge compensation was provided using low-energy electrons and low-energy Ar+ ions emission from the flood gun with a final calibration on adventitious carbon C1s peak (284.6 eV) as a reference. Spectral deconvolution was performed with the Avantage software provided by the manufacturer.
Mössbauer spectroscopy studies were done using the 57Fe gamma resonance transition. A Mössbauer system that consists of the Janis top-loaded liquid helium cryostat (Janis Research Company, Wilmington, MA 01887 USA) integrated with a conventional constant-acceleration spectrometer (Science Engineering & Education Co. USA) of the Kankeleit type in transmission geometry was used. During measurements, a 100 mCi Mössbauer 57Co(Rh) γ-ray source and the absorbers were kept at room temperature. The absorbers were made of fine pow- dered materials placed in thin-walled (~ 0.1 mm) cylindrical plastic containers. The used absorber thicknesses of about 10–12 mg/cm2 were calculated from the optimisation procedure38. The resonance 14.4 keV gamma
Scientific Reports |
(2021) 11:22746 |
https://doi.org/10.1038/s41598-021-01983-z
2

www.nature.com/scientificreports/
rays (for a given measurement and the energy scale calibration) were detected simultaneously by means of two independent LND Kr/CO2 proportional gas counters attached at opposite sides of the driving system. The drive velocity calibration was performed with a second 57Co(Rh) source against a standard metallic iron foil at room temperature. The Mössbauer spectra were analysed numerically by fitting a hyperfine parameter distribution (HPD) using the Voigt-line-based method of Rancourt and Ping39. In this method, the HPD for a given crystal site corresponding to similar structural, chemical, and magnetic properties is constructed by a sum of Gauss- ian components for the quadrupole splitting (QS) distributions and, if necessary, the magnetic hyperfine field Bhf distributions. The isomer shift (IS) can be linearly coupled to the primary hyperfine parameters (QS, Bhf).
For electrical measurement, all powders were hydraulically pressed into a pellet shape by applying the force of 4000 kg for 5 min. Calculated filling ratio of the measured palletized samples is: BFO = 50%, BLaFO = 55%, BEuFO = 49%, and for BErFO = 58%, thus these pellets are composed from ceramic and the air. Additionally, all pelletized samples were dried at 363 K in vacuum to eliminate the influence of humidity. An EDWARDS Auto 306 vacuum evaporator was used for deposition of 150 nm-thick gold electrodes onto both sides of the pellets to provide good contact between the sample and external electrodes during electrical measurements.
The electrical polarization loops of pelletized samples were recorded at room temperature with modified Sawyer–Tower circuit using a sinusoidal signal at 1 kHz frequency.
The dielectric response measurements were carried out using a Novocontrol GmbH Concept 80 broadband dielectric spectrometer equipped with a Quatro Cryosystem in the 10–1 ÷ 106 Hz frequency range and the tem- perature interval from 133 to 473 K with 10 K step.
The magnetic properties were measured using a Quantum Design MPMS-7 SQUID magnetometer. Full hysteresis loops were recorded up to a maximum field of 70 kOe at two temperatures: 300.0 K and 2.0 K. Solid samples were encapsulated in a Parafilm® M envelope, the mass of the sample was determined using a Sartorius SE2 ultramicroweight. The diamagnetic contribution from the envelope to the overall magnetisation was sub- tracted from databasing on the appropriately scaled magnetisation of the reference sample. Data analysis was carried out using the method of Corbellini et al.40, consisting of fitting the Voigt curve to the differentiated halves of the hysteresis curve. However, due to sparse number of experimental points at the low magnetic fields, the fit did not resemble the true nature of the samples. Thus, paramagnetic contributions were subtracted from the hysteresis loop using fitting of sum of Langevin-type curves. The procedure is elaborated in the Supplementary Information. Temperature-dependent magnetisation curves were registered in zero-field cooling/field cooling (ZFC/FC) experiments at 100.00 Oe. The temperature was swept between 310.0 and 2.0 K.
Results and discussion
Structural properties and composition. A detailed description of the synthesis procedure, analysis of crystalline phases, and morphology of bismuth ferrite doped with lanthanum, europium, or erbium are pre- sented in our previous work36. Herein, we have only provided a short description of the obtained data for a better understanding of our further results. The XRD patterns of the experimental samples are shown in Sup- plementary Information (Fig. S1). All powders have a fine microstructure with aggregated grains of different morphology36, characteristic for SCS-obtained materials28. The EDX analysis showed the elemental composition of nanopowders close to the stoichiometric one. According to an analysis of XRD data, synthesized materials are nanocrystalline powders of Bi0.9RE0.1FeO3 crystal phase with traces of Bi2Fe4O9 and Bi2O3 by-phases. Neverthe- less it should be underlined that all invastigated compounds exhibit content of the main phase, equal or higher than 90%36. The calculated average crystallite sizes of the main phases are 17 nm, 28 nm, 18 nm, and 18 nm for the neat BFO, BLaFO, BEuFO, and BErFO, respectively. Previously we found36, that the high-load doping of BFO with rare-earth ions leads to the distortion of its R3c crystal structure to an extent, which depends on the difference of ionic radii between the bismuth ion and corresponding rare-earth ion. In our case, the degree of distortion increases in a row BFO > BLaFO > BEuFO. Doping by Er3+ leads to a distortion of the crystal structure in a degree, which is high enough to promote the formation of two separate BiFeO3 phases: low-temperature rhombohedral R3c and orthorhombic Pbnm, metastable at room temperature.

XPS analysis. To study the near-to surface compositions of the experimental samples, high-resolution XPS spectra were recorded for each investigated sample in the Bi 4f, Fe 2p, O 1s, La 3d, Eu 3d, and Er 4p binding energy (BE) range (Fig. 1). The results of the peaks deconvolution are summarized in Table 1. Figure 1a shows the comparison of the XPS spectra recorded in the Bi 4f BE range for each investigated sample with superim- posed Bi 4f7/2 peaks used for spectral deconvolution. Each spectrum is composed of two peak doublets, with Bi 4f7/2 peaks located at 158.7 and 159.8 eV, respectively. The first and dominant of the two components is ascribed to bismuth in the BiFeO3 phase, while the latter one, may correspond to Bi2O3 oxide41–43.
The quantitative assessment of BiFeO3:Bi2O3 ratio, based on Bi 4f7/2 peak analysis, reveals that bismuth oxide share does not exceed 23% for undoped BFO, 30% for BLaFO and BEuFO, and 11% for BErFO. As XPS shows near to surface (5–10 nm deep) composition, while XRD could collect data up to 1 µm from surface, the differ- ence between bismuth oxide phase content measured by these two techniques suggests that the concentration of Bi2O3 is higher near to the surface regions. The observed phenomenon could be related to the higher influence of external factors, like atmosphere, moisture, and temperature gradient during synthesis and quenching, onto the layers of nanoparticles close to their surface. The Fe 2p signal from iron (Fig. 1b) also comes in two peak doublets, where Fe 2p3/2 peak corresponding to Fe2+ is located at 709.9 eV and Fe3+ at 711.9 eV43,44, with nearly equal stoichiometry for undoped BFO material. A slightly higher Fe3+ share was then recorded for both BEuFO and BLaFO samples, while the BErFO sample is characterized by a higher amount of lower valence Fe2+. The peaks for each additive are presented in Fig. 1d–f. Based on the XPS analysis and presence of La 3d5/2 peak at
837.1 eV, lanthanum is present within BLaFO as La3+, presumably in the form of La2O345 with a share of approx.
Scientific Reports |
(2021) 11:22746 |
https://doi.org/10.1038/s41598-021-01983-z
3

www.nature.com/scientificreports/
Figure 1. Deconvoluted high-resolution XPS spectra of the experimental samples in binding energy ranges of (a) Bi 4f, (b) Fe 2p, (c) O 1s, (d) La 3d5/2, (e) Eu 3d, (f) Er 4p3/2.
Table 1. The share of various chemical states of Bi, Fe, O, and rare-earth additives, based on high-resolution XPS analysis and spectral deconvolution. Results in at.%.
0.9 at.%. A similar observation is drawn for BEuFO, where europium is revealed as Eu3+ (Eu 3d5/2 at 1134.6 eV)46. The analysis of erbium was carried out within Er 4p3/2 BE range revealed a slightly smaller share of the element (0.5%), identified as Er3+47,48.
The spectra recorded in the O 1s BE range and shown in Fig. 1c reveal three XPS peaks. The first component, located at 529.5 eV, is characteristic of Fe–O interaction in Fe–O octahedron49 and corresponds to the O 1s core spectrum of bismuth ferrite lattice (OL)50,51. The peak at 530.7 eV is generally attributed to the chemisorbed oxygen caused by oxygen vacancies (Ov)50,51 or to Bi–O bonds in the BFO phase42,49. The low-intensity peak at
532.5 eV reveals C–O interaction. This signal could originate both from small traces of functionalized carbon, left in the samples as a result of incomplete fuel burning out52, and CO2 molecules, directly absorbed from the air. As the amount of carbon-containing phase is insignificant (not exceeding 7 at.% for each sample), its possible influence was excluded from consideration during further analyses. It is noticeable, that doping with rare-earth elements leads to the development of the peak located at 530.7 eV, implying either a higher share of Bi–O inter- action or the appearance of additional oxygen vacancies.
Based on the analysis of the presented XPS results we can conclude that each doped BFO sample reveals the altered chemistry of both Bi and Fe elements, where dopant addition tends to result in the appearance of more oxidized species with Eu and La doping, but more reduced species in the case of erbium. The combination of the influence of rare-earth doping elements with high-intense synthesis and post-synthesis temperature treatment conditions lead to a BFO phase degradation and split into near-to-surface regions of nanomaterials. However, we suppose, such a structure is not replicated in the bulk material. This leads to a formation of the inhomogene- ous structure, with BFO-rich inner core, and inhomogeneous outer layers, which consist of a mixture of oxides and non-stoichiometric BFO phases. The interaction of different layers, boundaries, and phases in the described complex structure could influence the properties of the BREFO nanopowders changing their electrical and magnetic surface- and bulk-related characteristics, as described in the text below.
Scientific Reports |
(2021) 11:22746 |
https://doi.org/10.1038/s41598-021-01983-z
4

Bi4f7/2
Fe2p3/2
O1s
Additive
BFO
Bi2O3
Fe2+
Fe3+
Fe–O
Bi-O
[Er/Eu/La]3+
BE/eV
158.7
159.8
709.9
711.9
529.5
530.7

BFO
18.6
5.7
4.3
4.4
41.2
25.8
–
BLaFO
16.6
7.0
2.8
4.3
34.0
34.4
0.9
BEuFO
17.4
7.5
3.5
5.2
35.0
30.5
0.9
BErFO
22.9
2.9
3.7
2.1
41.0
26.9
0.5

www.nature.com/scientificreports/
Figure 2. Room temperature 57Fe Mössbauer spectra of BiFeO3 and BiREFeO3.
Table 2. The hyperfine parameters obtained from the Mössbauer spectroscopy measurements at room temperature (IS—isomer shift, QS—quadrupole splitting, Bhf—magnetic hyperfine field). PM paramagnetic, HWHM Lorentzian linewidth.
57Fe Mössbauer spectroscopy. 57Fe Mössbauer spectra of the samples, obtained at room temperature, are pre- sented in Fig. 2. The hyperfine parameters of each component and their relative intensities received from the detailed numerical analysis of all spectra are listed in Table 2.
All recorded spectra have poor signal-to-noise ratio because of the very high absorption coefficient of bismuth for 14.4 keV gamma rays53, and interpretation of the results due to poor statistics should be taken with some caution. The room temperature spectra are close to symmetrical, however, the resonant lines are broadened (Table 2) relative to the instrumental linewidths of the calibration spectra.
Such broadening is caused by a distribution of QS, which indicates that not all crystallographic Fe-positions in the rhombohedral crystalline structure of BiFeO3 are completely equivalent. Moreover, the spectral asymmetry in BiFeO3 could also be caused by an incommensurate spin cycloid structure54–57.
All measured spectra are superposition of two components: (i) magnetic sextet related to perovskite-type structure of BiFeO3 (BiREFeO3) main phase (marked in red) and (ii) quadrupole doublet assigned to paramag- netic Bi2Fe4O9 impurity phase (marked in blue)56. The isomer shift of the main component is close to 0.3 mm/s, which is characteristic for high spin Fe3+. The magnetic hyperfine field of BiFeO3 is very close to the value reported by Palewicz et al.58. There is no significant change in the average magnetic hyperfine field (Bhf) values between Mössbauer spectra of BiFeO3 and rare-earth-doped BFO. This could indicate that the doping with the rare-earth elements leads to the replacement of bismuth in the A site of BiFeO3 crystal cell, and the number of magnetic nearest neighbors of Fe3+ remains the same56. It is worth noting that the most stable polymorph of iron oxides α-Fe2O3, which is a weak ferromagnet at room temperature, if present in our samples, should also result in a magnetic sextet. Thus, the relatively low value of Bhf ~ 49 T of the main magnetic phase indicates the absence of ferromagnetic α-Fe2O3 or any other unreacted iron oxide phases, which would have a much higher hyperfine
Scientific Reports |
(2021) 11:22746 |
https://doi.org/10.1038/s41598-021-01983-z
5
Sample
IS (mm s−1)
QS (mm s-1)
Bhf (T)
Area (%)
HWHM (mm/s)
Components
BFO
0.09
1.00
–
11
0.19
Fe3+ PM impurity
0.27
− 0.04
48.6(9)
89
Fe3+ magn. phase
BEuFO
0.20
0.87
–
24
0.20
Fe3+ PM impurity
0.30
− 0.04
49.0(7)
76
Fe3+ magn. phase
BErFO
0.24
0.84
–
11
0.20
Fe3+ PM impurity
0.29
− 0.05
48.8(6)
89
Fe3+ magn. phase
BLaFO
0.10
0.75
–
10
0.19
Fe3+ PM impurity
0.29
0.01
49.5(1.4)
90
Fe3+ magn. phase

www.nature.com/scientificreports/
Figure 3. Room temperature ferroelectric (P-E) hysteresis loop of BFO, BLaFO, BEuFO, and BErFO samples.
Table 3. The values of coercivity, remnant polarization, and saturation polarization for neat and doped BFO materials.
field up to 51.4 T59. On the other hand, a slight admixture of highly dispersed and oxidized magnetite cannot be completely excluded due to its much lower magnetic hyperfine field. The quadrupole splitting of the main com- ponent is close to zero, which is characteristic of the localization of Fe3+ ions near the center of FeO6 octahedra. The hyperfine interaction parameters of a doublet line are slightly different for all samples. However, they fall into the range of 0.09–0.24 mm/s for IS and 0.75–1.00 mm/s for QS. These values are similar to those reported for Bi2Fe4O955,57,60 and their dispersion, supposedly, originates from the low signal-to-noise ratio. Another possible origin for the quadrupole doublet is the nanoscale structure of BiFeO3 grains, which are small enough to become superparamagnetic. For instance, Park et al.9 showed similar Mössbauer parameters of the quadrupole doublet for 51 nm crystals of BiFeO3. In this case, it is almost impossible to distinguish the oxygen-deficient surrounding
of Fe2+ (or Fe3+) in low spin configuration from superparamagnetic BiFeO3 nanoparticles59.
Electrical properties. P‑E analysis. The correlation between polarization and the applied electric field at room temperature was studied using a modified Sawyer–Tower circuit. Ferroelectric hysteresis (P-E) loops of the neat and doped BiFeO3 are shown in Fig. 3.
Crucial parameters of ferroelectrics, such as remnant polarization (Pr), coercivity (Ec), and saturation polari- zation (Ps) were determined from the obtained hysteresis loops as shown in Table 3.
The ferroelectric properties of BFO materials are directly related to the orbital hybridization of Bi3+–O2– bonds. The narrow ferroelectric hysteresis loops of ferroelectric materials are characterized by a small amount of dis- sipated energy (low Ec) in repeatedly reversing polarization cycles.
Generally, it is difficult to obtain a saturated P-E loop for BFO ceramics due to leakage current caused by secondary phases and other defects, which can result in a partial reversal of the polarization. Taking into account samples’ porosity and the fact that investigated pallets are composed from ceramic nanoparticles the measured P-E loops exhibit unsaturated character. The increasing purity of the main BFO crystal phase could also contrib- ute to a decrease in leakage current61,62. The experimental samples have relatively low values of remnant polariza- tion and coercive field63,64, which indicates the existence of nano-sized ferroelectric domains and confirms the nano-specific character of the properties of studied materials.
However, despite the dominant influence of ferroelectric domains’ size, ferroelectric properties may also be affected by composition, homogeneity, and the presence and distribution of defects in nanomaterials65. We sup- pose the low value of ferroelectric parameters can be associated with the parasitic conductivity on grain bounda- ries and partially caused by impurity phases. Such conductivity is an intrinsic feature of magnetic compounds and often overlaps with the ferroelectric response of the multiferroic phase66. In BFO and BREFO compounds conductivity can be affected and contributed by electron transfer between localized ferric and ferrous ions, i.e. electron hopping between Fe3+ and Fe2+, morphology/microstructure and hopping of the oxygen vacancies that resembles the dipolar reorientation and results in a dielectric relaxation peak at high temperature67. Furthermore, the presence of Pbnm phase in erbium-doped BFO also leads to a decrease in the ferroelectric response of the samples due to symmetry constraints68.

Dielectric analysis. Temperature variation of the dielectric response of nanosized bismuth ferrites are described as rather complex and the results of the dielectric tests are presented in Fig. 4.
Scientific Reports |
(2021) 11:22746 |
https://doi.org/10.1038/s41598-021-01983-z
6
Parameter
BFO
BLaFO
BEuFO
BErFO
Coercivity (kV/cm)
0.17
0.61
0.75
0.59
Remnant polarization (nC/cm2)
11.43
8.20
30.39
7.77
Maximum polarization (saturation polarization) (nC/cm2)
76.32
17.27
48.53
16.69

www.nature.com/scientificreports/
Figure 4. Temperature and frequency dependence of the real part of dielectric permittivity of BFO, BLaFO, BEuFO, and BErFO samples.
Following Hunpratub et al. three temperature ranges could be distinguished on the εʹ vs. T spectra in BFO, which are characterized by different relaxation processes69: low-temperature dielectric relaxation (LTDR) in the range of ~ 133–293 K, middle-temperature dielectric relaxation (MTDR) at ~ 293–443 K, and high-temperature relaxation (HTDR) in the temperature range above ~ 443 K. In the case of studied compounds the border of mentioned processes is not well defined and difficult to distinguish. Also assignment of these relaxation pro- cesses is not easy and disputable. Nevertheless, according to Chybczyńska et al.70 the LTDR is related to the effect of mixed valence of the Fe ions, the MTDR attributed to grain boundary effect and the HTDR connecting to the ordering of oxygen vacancies. The analysis of measured dielectric response values and the nature of their change indicates that the dielectric response is associated with the intrinsic heterogeneity of the polycrystalline materials36,70 and agrees with XRD and XPS results (Figs. S1 and 1). As mentioned before, experimental powders consist of aggregated inhomogeneous nanograins of different sizes, forms, and features of the interconnection of grains and grain boundaries. It is known, that the grain boundaries and grain interiors show different electric conductivity. For instance, the conductivity of grain/crystallite boundaries in ferrites is connected to electron hopping Fe2+ – e– → Fe3+ among localized ferrous and ferric ions and significantly lower than that of the interior of the grains/crystallites70.

Magnetic properties. Figure 5 shows magnetisation hysteresis loops of the samples at 300.0 K and 2.0 K after subtraction of the paramagnetic contribution. Despite an elaborate model for hysteresis subtraction, the calculated and subtracted linear paramagnetic component at 300.0 K seems slightly overestimated, as the cor- rected magnetisation decreases in high magnetic fields. The results of the data analysis show that the magnetic properties of synthesized materials were significantly influenced by rare-earth doping. In the low magnetic field regime at 300.0 K, all samples exhibited similar behavior with ferromagnetic-like hysteresis and coercivity varying from 83.24 Oe for the BEuFO sample up to 127.04 Oe for the BLaFO sample. However, coercive fields decrease with the substitution of Bi3+ by smaller-sized Eu3+ and Er3+ ions. Such behavior could be related to dis- tortion and shrinkage of the BFO crystal cells36.
Subtraction of the paramagnetic component of M-H curves measured at 2.0 K resulted in a more reliable analysis of hysteresis, as the saturation observed in Fig. 5c is much more pronounced in the high magnetic field regime.
We found that the saturation magnetisation increases for all samples at 2.0 K in comparison with the satura- tion magnetisation values for the same samples at 300.0 K. The most significant increase was registered for neat BFO and Er3+-doped samples. The hysteresis loops obtained at 2.0 K exhibit a wasp-like shape. This can indicate that samples contain particles of a broad distribution of sizes with different values of coercivity71. The hysteresis loops at 2.0 K were successfully fitted using two superparamagnetic and one ferromagnetic Langevin-type curves as well as a term linear to the external magnetic field (the details described in the Supplementary Material). All calculated parameters of M-H curves are summarised in Table 4.
The observed saturation magnetisation of the neat BFO sample is notably higher than often reported in the literature. Huang et al.8 reported the saturation magnetisation of ferromagnetic part of the hysteresis loop of the sample containing 18 nm BFO particles to be around 0.13 emu/g at 300 K. At the same time, the authors showed that the highest saturation magnetisation of 0.15 emu/g was observed for BFO with nanoparticles of 62 nm8, which was ascribed to the structural anomaly emerging when the nanoparticle size approached the period of spiral-modulated spin structure. In a study by Park et al.9, the highest observed saturation magnetisation was estimated at 1.55 emu/g for 14 nm nanoparticles. Jayakumar et al.72 reported values smaller than 0.1 emu/g at
7.0 T without subtraction of significant paramagnetic components. However, there are several publications reporting saturation magnetisation in the same order of magnitude as our results. Verma and Kotnala73 found the saturation magnetisation at 300 K of their BFO at 4.73 emu/g, increasing up to 8.99 emu/g upon 10% doping with Pb. Tahir et al.74 showed the increase of room temperature saturation magnetisation from 9.202 emu/g for neat BFO to as high as 21.097 emu/g upon 30% doping with Ca.
Scientific Reports |
(2021) 11:22746 |
https://doi.org/10.1038/s41598-021-01983-z
7

www.nature.com/scientificreports/
Figure 5. (a) M-H curves of neat and doped BFO, measured at 300 K (coloured—filled symbols) and 2 K (black—open symbols), (b) enlarged M-H curves of neat and doped BFO measured at 300.0 K and (c) 2.0 K.
Table 4. Coercive field and the saturation magnetisation based on the fits.
The ZFC and FC (see Fig. S2) curves exhibit splitting that can be attributed to the coexistence of ferromagnetic and antiferromagnetic phases in the sample, a phenomenon known to happen for BiFeO38. The shape of the registered thermomagnetic curve is similar to that reported by Huang et al.8 for BiFeO3 nanoparticles of 83 nm in diameter, but with magnetisation values higher by a factor of about 100. Notably, the local maximum in the curves, interpreted as the spin-glass freezing temperature9, is not present in our data.
There are a few possible reasons for such discrepancy between most of the literature data and the experi- mental values obtained in this work. For instance, the concentration of oxygen vacancies in the structure of the obtained BFO was reported to influence the magnetisation of Dy-doped BFO75. The increasing number of oxygen vacancies could lead to the overall enhancement in the magnetisation of BFO-based nanomaterials, as it promotes an increase in the amount of Fe2+ to Fe3+ ions transitions for compensation of excess positive charge. The oxygen vacancies could also lead to an increased surface spin disorder by uncompensated spins from Fe3+ ions. Another possible reason is that saturation magnetisation could increase due to the distortion of the crystal structure of nanograins. A decrease in crystallite size increases the influence of uncompensated surface spins with increased contribution of the uncompensated ferromagnetic surface layers to ferromagnetic components of magnetisation9,76. Simultaneously, smaller crystalline sizes of BFO nanomaterials are related to a suppression of spiral spin order and higher shape anisotropy. Both factors were reported to have a significant influence on the ferromagnetism of BFO-based nanomaterials9,77. At the same time, rare-earth doping could induce an increase in the canting angle of layers due to the tilt of FeO6 octahedra78, which even further increases the overall magnetisa- tion. And last but not the least, magnetisation is highly sensitive to impurities and phase inhomogeneity. As it was shown previously by XRD and XPS analysis, the experimental samples contain Bi2Fe4O9 and Bi2O3 by-phases with a different magnetization behavior79–81, which form inhomogeneous structures in combination with BFO and BReFO phases. However, despite significant paramagnetic-like components, the saturation magnetisation of the ferromagnetic part of the reported hysteresis loop for Bi2Fe4O9 was not higher than 0.3 emu/g. Based on this fact we could conclude the presence of the Bi2Fe4O9 phase at the estimated concentration cannot be responsible for the observed magnetisation values. Diamagnetic bismuth(III) oxide82 could only add to the linear term of the hysteresis loop but would not affect saturation values. As the saturation magnetisation of Fe3O4 is estimated at 98 emu/g83, some impurities as low as 5% would be sufficient to explain the value of the observed saturation magnetisation. This hypothesis can be supported by the considerable share of Fe(II) species in comparison to
Scientific Reports |
(2021) 11:22746 |
https://doi.org/10.1038/s41598-021-01983-z
8
Sample
Temperature (K)
Coercivity of the sample (Oe)
Coercivity of the ferromagnetic component (Oe)
Saturation magnetisation of the ferromagnetic component (emu/g)
BFO
300.0
108.19
124.3 ± 1.3
4.593 ± 0.060
2.0
336.41
555.8 ± 7.9
10.45 ± 0.43
BLaFO
300.0
127.04
133.4 ± 2.0
5.161 ± 0.082
2.0
381.95
487.3 ± 5.2
5.834 ± 0.092
BEuFO
300.0
83.24
107.7 ± 5.0
4.886 ± 0.085
2.0
268.34
536.0 ± 21
6.13 ± 0.24
BErFO
300.0
98.06
115.5 ± 3.4
4.026 ± 0.084
2.0
86.6
490.0 ± 17
12.07 ± 0.16

www.nature.com/scientificreports/
Fe(III) species, evidenced by XPS measurements. At the same time, however, the results of XRD analysis and Mössbauer spectroscopy do not expose the presence of any significant amount of iron oxide magnetic species, regardless of whether ferromagnetic or superparamagnetic. This fact leads us to the conclusion that even if there are some other than BFO magnetic phases in the samples contributing to the overall magnetisation, they would not be a significant part of the sample mass.
Conclusions
In this study, a series of Bi0.9RE0.1FeO3 (RE = La, Eu, and Er) powders was prepared by the SCS method and their structural features, and factors that influence nanomaterials electric, and magnetic properties were carefully studied and analysed.
1.
The results of XRD, XPS, and Mössbauer spectroscopy analyses revealed that all obtained materials are nanocrystalline powders with predominantly BFO or modified BREFO nanograins and thin outer layers enriched with Bi2Fe4O9, Bi2O3, and rare-earth metal oxides. The formation of an inhomogeneous structure was associated with the unequal influence of the external atmosphere and temperature gradient during synthesis and post-synthesis quenching.
The electrical measurements confirmed the ferroelectric behaviour of neat and RE-doped BFO with the presence of spontaneous polarization.
It was found, the synthesized materials are characterized with significantly improved magnetic properties, which are related to the structural transformation, promoted by the RE doping. At the same time, the analyses showed a decrease in coercive fields with the substitution of Bi3+ by smaller-sized Eu3+ and Er3+ ions due to the distortion of the crystal cells and volume shrinkage.
All the studied materials are characterized by relatively high values of magnetisation and coercivity. The highest measured values of saturation magnetisation of the ferromagnetic component (5.161 emu/g) and coercivity (133.4 Oe) among all the studied materials at 300.0 K are found for the Bi0.9La0.1FeO3 nanopowder. The main contribution to the magnetic behaviour of the nanopowders was associated with the BFO-based phase, as the presence of a significant amount of iron oxides or any other ferromagnetic phases were excluded by XRD and Mössbauer spectroscopy.
Based on the data analysis we concluded, the possible explanations for so high magnetic properties are
(i) the influence of oxygen vacancies in the structure of the obtained BFO, supported by the presence of high-temperature dielectric relaxations in the broadband dielectric spectroscopy spectra; and (ii) nanosized structural parameters of crystallites, supported by narrow ferroelectric hysteresis loops.
The results of the study showed that SCS is a promising method for the preparation of a broad variety of neat and doped BFO-based nanomaterials with enhanced magnetic properties. Overall the SCS-obtained BFO-based materials are promising candidates for application as components of various electronic devices. The same SCS approach could also be used for the synthesis of other types of ferromagnetic nanomaterials with enhanced properties.
2.
3.
4.
5.
6.
Received: 16 August 2021; Accepted: 8 November 2021
References
1. Catalan, G. & Scott, J. F. Physics and applications of bismuth ferrite. Adv. Mater. 21, 2463–2485. https://doi.org/10.1002/adma. 200802849 (2009).
2. Reddy, B. P., Sekhar, M. C., Prakash, B. P., Suh, Y. & Park, S. Photocatalytic, magnetic, and electrochemical properties of La doped BiFeO3 nanoparticles. Ceram. Int. 44, 19512–19521. https://doi.org/10.1016/j.ceramint.2018.07.191 (2018).
3. Kubel, F. & Schmid, H. Structure of a ferroelectric and ferroelastic monodomain crystal of the perovskite BiFeO3. Acta Crystallogr. Sect. B 46, 698–702. https://doi.org/10.1107/S0108768190006887 (1990).
4. Sosnowska, I., Neumaier, T. P. & Steichele, E. Spiral magnetic ordering in bismuth ferrite. J. Phys. C Solid State Phys. 15, 4835–4846. https://doi.org/10.1088/0022-3719/15/23/020 (1982).
5. Dzyaloshinsky, I. A thermodynamic theory of gadolinium molybdate. J. Phys. Chem. Solids 4, 241–255. https://doi.org/10.1016/ 0022-3697(58)90076-3 (1958).
6. Treves, D. & Alexander, S. Observation of antisymmetric exchange interaction in yttrium orthoferrite. J. Appl. Phys. 33, 1133–1134. https://doi.org/10.1063/1.1728631 (1962).
7. Riaz, S., Shah, S. M. H., Akbar, A., Kayani, Z. N. & Naseem, S. Effect of Bi/Fe ratio on the structural and magnetic properties of BiFeO3 thin films by sol-gel. IEEE Trans. Magn. 50, 2–5. https://doi.org/10.1109/TMAG.2014.2313002 (2014).
8. Huang, F. et al. Peculiar magnetism of BiFeO3 nanoparticles with size approaching the period of the spiral spin structure. Sci. Rep.
3, 1–7. https://doi.org/10.1038/srep02907 (2013).
1. Park, T. J., Papaefthymiou, G. C., Viescas, A. J., Moodenbaugh, A. R. & Wong, S. S. Size-dependent magnetic properties of single- crystalline multiferroic BiFeO3 nanoparticles. Nano Lett. 7, 766–772. https://doi.org/10.1021/nl063039w (2007).
2. Kalinkin, A. N., Kozhbakhteev, E. M., Polyakov, A. E. & Skorikov, V. M. Application of BiFeO3 and Bi4Ti3O12 in ferroelectric memory, phase shifters of a phased array, and microwave HEMTs. Inorg. Mater. 49, 1031–1043. https://doi.org/10.1134/S0020 168513100038 (2013).
3. Bibes, M. & Barthélémy, A. Towards a magnetoelectric memory. Nat. Mater. 7, 425–426. https://doi.org/10.1038/nmat2189 (2008).
4. Rhaman, M. M., Matin, M. A., Hakim, M. A. & Islam, M. F. Bandgap tuning of samarium and cobalt co-doped bismuth ferrite nanoparticles. Mater. Sci. Eng. B Solid‑State Mater. Adv. Technol. 263, 114842. https://doi.org/10.1016/j.mseb.2020.114842 (2021).
5. Bala, A., Majumder, S. B., Dewan, M. & Roy Chaudhuri, A. Hydrogen sensing characteristics of perovskite based calcium doped BiFeO3 thin films. Int. J. Hydrogen Energy 44, 18648–18656. https://doi.org/10.1016/j.ijhydene.2019.05.076 (2019).
6. Dai, Z., Fujita, Y. & Akishige, Y. Dielectric properties and heating effect of multiferroic BiFeO3 suspension. Mater. Lett. 65, 2036–2038. https://doi.org/10.1016/j.matlet.2011.04.029 (2011).
Scientific Reports |
(2021) 11:22746 |
https://doi.org/10.1038/s41598-021-01983-z
9

www.nature.com/scientificreports/
1. Gao, F. et al. Visible-light photocatalytic properties of weak magnetic BiFeO3 nanoparticles. Adv. Mater. 19, 2889–2892. https:// doi.org/10.1002/adma.200602377 (2007).
2. Xiong, Z. & Cao, L. Tailoring morphology, enhancing magnetization and photocatalytic activity via Cr doping in Bi25FeO40. J. Alloys Compd. 773, 828–837. https://doi.org/10.1016/j.jallcom.2018.09.344 (2019).
3. Abdul Satar, N. S. et al. Facile green synthesis of ytrium-doped BiFeO3 with highly efficient photocatalytic degradation towards methylene blue. Ceram. Int. 45, 15964–15973. https://doi.org/10.1016/j.ceramint.2019.05.105 (2019).
4. Lin, Y., Wang, Q., Gao, S., Yang, H. & Liu, P. Morphology-controlled porous Bi0.9La0.1FeO3 microspheres for applications in super- capacitors. Ceram. Int. 44, 2649–2655. https://doi.org/10.1016/j.ceramint.2017.10.064 (2018).
5. Ankur, S. N., Nanda, S. J., Mamraj, C. M., Debananda, S. & Rahul, M. Sol–gel synthesized—BiFeO3–graphene nanocomposite as efficient electrode for supercapacitor application. J. Mater. Sci. Mater. Electron. 29, 9361–9368. https://doi.org/10.1007/s10854- 018-8967-6 (2018).
6. Valant, M., Axelsson, A.-K. & Alford, N. Peculiarities of a solid-state synthesis of multiferroic polycrystalline BiFeO3. Chem. Mater.
19, 5431–5436. https://doi.org/10.1021/cm071730+ (2007).
1. Arnold, D. Composition-driven structural phase transitions in rare-earth-doped bifeo3 ceramics: A review. IEEE Trans. Ultrason. Ferroelectr. Freq. Control 62, 62–82. https://doi.org/10.1109/TUFFC.2014.006668 (2015).
2. Hong, Y. et al. Effect of octahedron tilt on the structure and magnetic properties of bismuth ferrite. J. Adv. Ceramics. 9, 641–646. https://doi.org/10.1007/s40145-020-0398-1 (2020).
3. Golda, R. A., Marikani, A. & Alex, E. J. Enhancement of dielectric, ferromagnetic and electrochemical properties of BiFeO3 nanostructured films through rare earth metal doping. Ceram. Int. 46, 1962–1973. https://doi.org/10.1016/j.ceramint.2019.09. 175 (2020).
4. Rojas-George, G., Solís-Canto, O., Esparza-Ponce, H. E. & Reyes-Rojas, A. Multiferroic response in bismuth ferrite doped hetero- structures: A buffer layer inference. Appl. Surf. Sci. 533, 147491. https://doi.org/10.1016/j.apsusc.2020.147491 (2020).
5. Perdomo, C. P. F., Suarez, A. V., Gunnewiek, R. F. K. & Kiminami, R. H. G. A. Low temperature synthesis of high purity nanoscaled BiFeO3 by a fast polymer solution method and their ferromagnetic behavior. J. Alloys Compd. 849, 156564. https://doi.org/10. 1016/j.jallcom.2020.156564 (2020).
6. Asefi, N., Masoudpanah, S. M. & Hasheminiasari, M. Photocatalytic performances of BiFeO3 powders synthesized by solution combustion method: The role of mixed fuels. Mater. Chem. Phys. 228, 168–174. https://doi.org/10.1016/j.matchemphys.2019.02. 059 (2019).
7. Li, F. T., Ran, J., Jaroniec, M. & Qiao, S. Z. Solution combustion synthesis of metal oxide nanomaterials for energy storage and conversion. Nanoscale 7, 17590–17610. https://doi.org/10.1039/c5nr05299h (2015).
8. Varma, A., Mukasyan, A. S., Rogachev, A. S. & Manukyan, K. V. Solution combustion synthesis of nanoscale materials. Chem. Rev.
116, 14493–14586. https://doi.org/10.1021/acs.chemrev.6b00279 (2016).
1. Novitskaya, E., Kelly, J. P., Bhaduri, S. & Graeve, O. A. A review of solution combustion synthesis: An analysis of parameters controlling powder characteristics. Int. Mater. Rev. https://doi.org/10.1080/09506608.2020.1765603 (2020).
2. Sdobnyakov, N. et al. Solution combustion synthesis and Monte Carlo simulation of the formation of CuNi integrated nanoparticles.
Comput. Mater. Sci. 184, 109936. https://doi.org/10.1016/j.commatsci.2020.109936 (2020).
1. Khort, A., Podbolotov, K., Serrano-García, R. & Gun’ko, Y. K. One-step solution combustion synthesis of pure Ni nanopowders with enhanced coercivity: The fuel effect. J. Solid State Chem. 253, 270–276. https://doi.org/10.1016/j.jssc.2017.05.043 (2017).
2. Khort, A. et al. Graphene@metal nanocomposites by solution combustion synthesis. Inorg. Chem. 59, 6550–6565. https://doi.org/ 10.1021/acs.inorgchem.0c00673 (2020).
3. Lakshmiprasanna, H. R. et al. Effect of Pr3+-doping on the structural, elastic and magnetic properties of Mn–Zn ferrite nanopar- ticles prepared by solution combustion synthesis method. Chem. Data Collect. 24, 100273. https://doi.org/10.1016/j.cdc.2019. 100273 (2019).
4. Khort, A. A. & Podbolotov, K. B. Preparation of BaTiO3 nanopowders by the solution combustion method. Ceram. Int. 42, 15343–15348. https://doi.org/10.1016/j.ceramint.2016.06.178 (2016).
5. Zhou, J., Jiang, L. & Chen, D. Facile synthesis of Er-doped BiFeO3 nanoparticles for enhanced visible light photocatalytic degrada- tion of tetracycline hydrochloride. J. Sol‑Gel Sci. Technol. 90, 535–546. https://doi.org/10.1007/s10971-019-04932-5 (2019).
6. Wrzesinska, A., Khort, A., Bobowska, I., Busiakiewicz, A. & Wypych-Puszkarz, A. Influence of the La3+, Eu3+, and Er3+ doping on structural, optical, and electrical properties of BiFeO3 nanoparticles synthesized by microwave-assisted solution combustion method. J. Nanomater. https://doi.org/10.1155/2019/5394325 (2019).
7. Shannon, R. D. Revised effective ionic radii and systematic studies of interatomie distances in halides and chaleogenides. Acta Crystallogr. Sect. A Found. Adv. 32, 751–767. https://doi.org/10.1107/S0567739476001551 (1976).
8. Long, G. J., Cranshaw, T. E. & Longworth, G. The ideal Mössbauer effect absorber thickness. Mössbauer Eff. Ref. Data J. 6, 42–49 (1983).
9. Rancourt, D. G. & Ping, J. Y. Voigt-based methods for arbitrary-shape static hyperfine parameter distributions in Mössbauer spectroscopy. Nucl. Inst. Methods Phys. Res. B 58, 85–97. https://doi.org/10.1016/0168-583X(91)95681-3 (1991).
10. Corbellini, L. et al. Hysteresis loops revisited: An efficient method to analyze ferroic materials. J. Appl. Phys. 120, 124101. https:// doi.org/10.1063/1.4963756 (2016).
11. Wang, X., Fan, J., Qian, F. & Min, Y. Magnetic BiFeO3 grafted with MWCNT hybrids as advanced photocatalysts for removing organic contamination with a high concentration. RSC Adv. 6, 49966–49972. https://doi.org/10.1039/c6ra08316a (2016).
12. Han, S. & Sung Kim, C. Weak ferromagnetic behavior of BiFeO3 at low temperature. J. Appl. Phys. 113, 48–51. https://doi.org/10. 1063/1.4801338 (2013).
13. Chybczyńska, K. et al. Synthesis and properties of bismuth ferrite multiferroic flowers. J. Mater. Sci. 49, 2596–2604. https://doi. org/10.1007/s10853-013-7957-6 (2014).
14. Yamashita, T. & Hayes, P. Analysis of XPS spectra of Fe2+ and Fe3+ ions in oxide materials. Appl. Surf. Sci. 254, 2441–2449. https:// doi.org/10.1016/j.apsusc.2007.09.063 (2008).
15. Gaikwad, V. M. et al. Design of process for stabilization of La2NiMnO6 nanorods and their magnetic properties. J. Magn. Magn. Mater. 492, 165652. https://doi.org/10.1016/j.jmmm.2019.165652 (2019).
16. Pietrzak, T. K. et al. Photoluminescence of partially reduced Eu2+/Eu3+ active centers in a NaF–Al2O3–P2O5 glassy matrix with tunable smooth spectra. J. Lumin. 208, 322–326. https://doi.org/10.1016/j.jlumin.2018.12.060 (2019).
17. Khosla, R. & Sharma, S. K. Frequency dispersion and dielectric relaxation in postdeposition annealed high-κ erbium oxide metal– oxide–semiconductor capacitors. J. Vac. Sci. Technol. B Nanotechnol. Microelectron. Mater. Process. Meas. Phenom. 36, 012201. https://doi.org/10.1116/1.4995809 (2018).
18. Sedik, A. et al. Characterization of TiO2 films obtained by a wet chemical process. J. Electr. Eng. 68, 31–36. https://doi.org/10.1515/ jee-2017-0052 (2017).
19. Mukherjee, A., Chakrabarty, S., Kumari, N., Su, W. N. & Basu, S. Visible-light-mediated electrocatalytic activity in reduced graphene oxide-supported bismuth ferrite. ACS Omega 3, 5946–5957. https://doi.org/10.1021/acsomega.8b00708 (2018).
20. Das, R., Sarkar, T. & Mandal, K. Multiferroic properties of Ba2+ and Gd3+ co-doped bismuth ferrite: Magnetic, ferroelectric and impedance spectroscopic analysis. J. Phys. D. Appl. Phys. 45, 455002. https://doi.org/10.1088/0022-3727/45/45/455002 (2012).
21. Di, L., Yang, H., Xian, T. & Chen, X. Enhanced photocatalytic activity of NaBH4 reduced BiFeO3 nanoparticles for rhodamine B decolorization. Materials 10, 1–11. https://doi.org/10.3390/ma10101118 (2017).
Scientific Reports |
(2021) 11:22746 |
https://doi.org/10.1038/s41598-021-01983-z
10

www.nature.com/scientificreports/
1. Khort, A., Romanovski, V., Leybo, D. & Moskovskikh, D. CO oxidation and organic dyes degradation over graphene–Cu and gra- phene–CuNi catalysts obtained by solution combustion synthesis. Sci. Rep. 10, 1–10. https://doi.org/10.1038/s41598-020-72872-0 (2020).
2. Blaauw, C. & van der Woude, F. Magnetic and structural properties of interfaces. J. Phys. C Solid State Phys. 6, 1422–1431. https:// doi.org/10.1007/BF02146301 (1973).
3. Sobolev, A. et al. Mössbauer investigations of hyperfine interactions features of 57Fe nuclei in BiFeO3 ferrite. AIP Conf. Proc. 1622, 104–108. https://doi.org/10.1063/1.4898617 (2014).
4. Liu, G. et al. Mossbauer studies of BiFeO3 mulitiferroic nanoparticles doped with Eu. Hyperfine Interact. 241, 2–7. https://doi.org/ 10.1007/s10751-020-01709-z (2020).
5. Kothari, D., Reddy, V. R., Gupta, A., Meneghini, C. & Aquilanti, G. Eu doping in multiferroic BiFeO3 ceramics studied by Moss- bauer and EXAFS spectroscopy. J. Phys. Condens. Matter 22, 356001. https://doi.org/10.1088/0953-8984/22/35/356001 (2010).
6. Pierzga, A. et al. Orientation of the electric field gradient and ellipticity of the magnetic cycloid in multiferroic BiFeO3. Philos. Mag. 97, 168–174. https://doi.org/10.1080/14786435.2016.1248518 (2017).
7. Palewicz, A., Szumiata, T., Przeniosło, R., Sosnowska, I. & Margiolaki, I. Search for new modulations in the BiFeO3 structure: SR diffraction and Mössbauer studies. Solid State Commun. 140, 359–363. https://doi.org/10.1016/j.ssc.2006.08.046 (2006).
8. Jartych, E., Malesa, B., Antolak-Dudka, A. & Oleszak, D. Mössbauer spectroscopy studies of multiferroic (BiFeO3)1–x-(BaTiO3)x solid solutions prepared by mechanical activation. Acta Phys. Pol. A 125, 837–839. https://doi.org/10.12693/APhysPolA.125.837 (2014).
9. Prado-Gonjal, J. et al. Structural, microstructural and Mössbauer study of BiFeO3 synthesized at low temperature by a microwave- hydrothermal method. Solid State Sci. 13, 2030–2036. https://doi.org/10.1016/j.solidstatesciences.2011.09.006 (2011).
10. Sharma, S., Singh, V., Kotnala, R. K. & Dwivedi, R. K. Comparative studies of pure BiFeO3 prepared by sol–gel versus conventional solid-state-reaction method. J Mater. Sci. Mater. Electron. https://doi.org/10.1007/s10854-014-1820-7 (2014).
11. Sree, C. et al. Electrical and magnetic properties of nanocrystalline BiFeO3 prepared by high energy ball milling and microwave sintering. J. Nanosci. Nanotechnol. 11, 4097–4102. https://doi.org/10.1166/jnn.2011.3852 (2011).
12. Yin, R.-Q. et al. Pure-phase BiFeO3 ceramics with enhanced electrical properties prepared by two-step sintering. Ceram. Int. 43, 6467–6471. https://doi.org/10.1016/j.ceramint.2017.02.063 (2017).
13. Yao, Y., Liu, W., Chan, Y., Leung, C. & Mak, C. Studies of rare-earth-doped BiFeO3 ceramics. Int. J. Appl. Ceram. Technol. 1253, 1246–1253. https://doi.org/10.1111/j.1744-7402.2010.02577.x (2011).
14. Jiang, B. et al. Barium titanate at the nanoscale: Controlled synthesis and dielectric and ferroelectric properties. Chem. Soc. Rev.
48, 1194–1228. https://doi.org/10.1039/c8cs00583d (2019).
1. Wang, Y. P. et al. Room-temperature saturated ferroelectric polarization in BiFeO3 ceramics synthesized by rapid liquid phase sintering. Appl. Phys. Lett. 84, 1731–1733. https://doi.org/10.1063/1.1667612 (2004).
2. Markiewicz, E., Hilczer, B., Błaszyk, M., Pietraszko, A. & Talik, E. Dielectric properties of BiFeO3 ceramics obtained from mecha- nochemically synthesized nanopowders. J. Electroceramics 27, 154–161. https://doi.org/10.1007/s10832-011-9660-9 (2011).
3. Tylczyński, Z. A collection of 505 papers on false or unconfirmed ferroelectric properties in single crystals, ceramics and polymers.
Front. Phys. 14, 63301. https://doi.org/10.1007/s11467-019-0912-5 (2019).
1. Hunpratub, S., Thongbai, P., Yamwong, T., Yimnirun, R. & Maensiri, S. Dielectric relaxations and dielectric response in multiferroic ceramics. Appl. Phys. Lett. 94, 062904. https://doi.org/10.1063/1.3078825 (2009).
2. Chybczyńska, K., Markiewicz, E., Błaszyk, M., Hilczer, B. & Andrzejewski, B. Dielectric response and electric conductivity of ceramics obtained from BiFeO3 synthesized by microwave hydrothermal method. J. Alloys Compd. 671, 493–501. https://doi.org/ 10.1016/j.jallcom.2016.02.104 (2016).
3. Iorgu, A. I. et al. Fast synthesis of rare-earth (Pr3+, Sm3+, Eu3+ and Gd3+) doped bismuth ferrite powders with enhanced magnetic properties. J. Alloys Compd. 629, 62–68. https://doi.org/10.1016/j.jallcom.2014.12.108 (2015).
4. Jayakumar, O. D. et al. Theoretical and experimental evidence of enhanced ferromagnetism in Ba and Mn cosubstituted BiFeO3.
Appl. Phys. Lett. 96, 10–13. https://doi.org/10.1063/1.3280043 (2010).
1. Verma, K. C. & Kotnala, R. K. Tailoring the multiferroic behavior in BiFeO3 nanostructures by Pb doping. RSC Adv. 6, 57727–57738. https://doi.org/10.1039/c6ra12949h (2016).
2. Tahir, M. et al. Enhanced structural and magnetic ordering in as-synthesized Ca doped bismuth iron oxide nanoceramics. J. Alloys Compd. 832, 154725. https://doi.org/10.1016/j.jallcom.2020.154725 (2020).
3. Liu, R. et al. Oxygen-vacancy-controlled magnetic properties with magnetic pole inversion in BiFeO3-based multiferroics. J. Am. Ceram. Soc. 103, 1097–1104. https://doi.org/10.1111/jace.16789 (2020).
4. Annapu Reddy, V., Pathak, N. P. & Nath, R. Particle size dependent magnetic properties and phase transitions in multiferroic BiFeO3 nano-particles. J. Alloys Compd. 543, 206–212. https://doi.org/10.1016/j.jallcom.2012.07.098 (2012).
5. Hasan, M., Islam, M. F., Mahbub, R., Hossain, M. S. & Hakim, M. A. A soft chemical route to the synthesis of BiFeO3 nanoparticles with enhanced magnetization. Mater. Res. Bull. 73, 179–186. https://doi.org/10.1016/j.materresbull.2015.09.007 (2016).
6. Liu, Y. Q. et al. Effect of Ho substitution on structure and magnetic property of BiFeO3 prepared by sol-gel method. Mater. Sci. Semicond. Process. 40, 787–795. https://doi.org/10.1016/j.mssp.2015.06.090 (2015).
7. Lavasani, S. A. N. H., Mirzaee, O., Shokrollahi, H., Moghadam, A. K. & Salami, M. Magnetic and morphological characterization of Bi2Fe4O9 nanoparticles synthesized via a new reverse chemical co-precipitation method. Ceram. Int. 43, 12120–12125. https:// doi.org/10.1016/j.ceramint.2017.06.069 (2017).
8. Zhang, M. et al. Polyacrylamide gel synthesis and photocatalytic performance of Bi2Fe4O9 nanoparticles. J. Alloys Compd. 509, 809–812. https://doi.org/10.1016/j.jallcom.2010.09.097 (2011).
9. Kharkovskii, A. I., Nizhankovskii, V. L., Kravchenko, E. A. & Orlov, V. G. Magnetic properties of the bismuth oxide α-Bi2O3.
Zeitschrift für Naturforsch. A 51, 665–666. https://doi.org/10.1515/zna-1996-5-649 (1996).
1. Madelung, O., Rössler, U. & Schulz, M. Bismuth oxide (Bi2O3) magnetic properties. In Non‑Tetrahedrally Bonded Elements and Binary Compounds I 1–2 (Springer, 1998).
2. Guardia, P., Labarta, A. & Batlle, X. Tuning the size, the shape, and the magnetic properties of iron oxide nanoparticles. J. Phys. Chem. C 115, 390–396. https://doi.org/10.1021/jp1084982 (2011).
Acknowledgements
The equipment used for SQUID magnetometry was sponsored in part by the Centre for Preclinical Research and Technology (CePT), a project co-sponsored by European Regional Development Fund and Innovative Economy, The National Cohesion Strategy of Poland. The authors gratefully acknowledge Prof. Abílio Almeida (Polarizable Materials and Functional Nanostructures Group, Material Physics Institute, University of Porto) for performing ferroelectric measurements. The authors also gratefully acknowledge financial support the Ministry of Science and Higher Education of the Russian Federation in the framework of Increase Competitiveness Program of NUST
«MISiS» (K2-2020-024), implemented by a governmental decree dated 16th of March 2013, N 211.
Scientific Reports |
(2021) 11:22746 |
https://doi.org/10.1038/s41598-021-01983-z
11

www.nature.com/scientificreports/
Author contributions
A.W.: Conceptualization, formal analysis, investigation, writing—original draft; A.K.: formal analysis, investiga- tion, writing—original draft; M.W., J.R., J.G.: investigation, formal analysis, writing—original draft; JS: supervi- sion, funding acquisition; D.S.K.: investigation; writing—review and editing; K.Ł., T.S.: formal analysis, supervi- sion; A.W-P.: conceptualization, formal analysis, writing—original draft, supervision.
Funding
Open access funding provided by Royal Institute of Technology.
Competing interests
The authors declare no competing interests.
Additional information
Supplementary Information The online version contains supplementary material available at https://doi.org/ 10.1038/s41598-021-01983-z.
Correspondence and requests for materials should be addressed to A.W. or A.K.
Reprints and permissions information is available at www.nature.com/reprints.
Publisher’s note Springer Nature remains neutral with regard to jurisdictional claims in published maps and institutional affiliations.
Open Access This article is licensed under a Creative Commons Attribution 4.0 International
License, which permits use, sharing, adaptation, distribution and reproduction in any medium or
format, as long as you give appropriate credit to the original author(s) and the source, provide a link to the
Creative Commons licence, and indicate if changes were made. The images or other third party material in this article are included in the article’s Creative Commons licence, unless indicated otherwise in a credit line to the material. If material is not included in the article’s Creative Commons licence and your intended use is not permitted by statutory regulation or exceeds the permitted use, you will need to obtain permission directly from the copyright holder. To view a copy of this licence, visit http://creativecommons.org/licenses/by/4.0/.
© The Author(s) 2021
Scientific Reports |
(2021) 11:22746 |
https://doi.org/10.1038/s41598-021-01983-z
12