J Therm Anal Calorim (2014) 118:1049–1056 DOI 10.1007/s10973-014-3803-6
Thermal properties of polycrystalline[Mn(NH3)6](ClO4)2
Crystal structure and phasetransitions
JoannaHetman´czyk•ŁukaszHetman´czyk•
Anna Migdał-Mikuli•Edward Mikuli
Received: 1 November 2013 / Accepted: 27 March 2014 / Published online: 27 April 2014
©The Author(s) 2014. This article is published with open access at Springerlink.com
Abstract The X-ray powder diffraction (XRPD) pattern of [Mn(NH3)6](ClO4)2at room temperature can be indexed in the regular (cubic) system (Fm3m space group)with
latticecellparametera=11.5729A˚andwithfourmole-
cules per unit cell. The XRPD pattern at 100 K is evidently different, and it indicates lowering of the crystal structure.
Introduction
Alluptonowinvestigatedioniccoordinationcompoundsofthetype[M(NH3)6](ClO4)2,whereM=Mg2?,Ca2?,Fe2?,
Co2?,
Ni2?
Cd2?
and
posses similar and very specific
polymorphism[1–6].Allofthemownedcubicsymmetryof the crystal lattice (Fm3m) of the high (room) temperature phase [7]. Phase transition atTC1, connected with thelargeentropy change, was connected with the change of the crystal structure (mainly to the monoclinic phase; space group P21/c) and also with a drastic change of the speedof
One phase transition atTh=143.5 K (on heating) and at
C1
=137.6 K (on cooling) was detected by DSC for
Tc
C1
[Mn(NH3)6](ClO4)2in the range of 120–300 K. The fol-
lowingthermodynamicparametersforphaseI$phaseII
transitionwereobtained:DH=3.1±0.2kJmol-1andDS=21.6±0.3Jmol-1K-1.Thelargevalueofentropychanges (DS) indicates considerable configurational disor-der in the high temperature phase. The presence of 5.9K hysteresis of the phase transition temperature atTCand sharpnessoftheheatflowanomalyattestthatthedetected phasetransitionisofthefirst-ordertype.Appearingofthe twonewbands(splittingofds(HNH)F1umode)inFT-MIRspectraatthevicinityof1200cm-1suggeststhatthephasetransition undergoes a change of the crystalstructure.
reorientationalmotionsofClO-anions[1,8,9].Itwas
4
thought interesting to see whether a compound of the same type but with different cationsM= Mn2?will possess a structure at room temperature and a phase polymorphism similartothatofthosecompoundsjustmentioned.Sofar,no data have been available about the crystal structure of [Mn(NH3)6](ClO4)2. Our results of X-ray investigations (XRDP)ofthecrystalstructureofinvestigatedcompoundin the room temperature (RT) phase are presented inResultsand discussionof this paper.
The general aim of the present study is to investigate the polymorphism of [Mn(NH3)6](ClO4)2in the temper- ature range of 120–300 K and find the connections of recorded phase transitions with eventual changes of the crystal structure. For this purpose, we employed besides XRPD also Fourier transforms middle-infrared spectros- copy (FT-MIR). In addition, we would like to obtain a better understanding of mechanisms of thermal decom- position of the title compound, particularly of its deam- mination processes. The results of thermal analysis of [Mn(NH3)6](ClO4)2have been described in the literature [10]. It undergoes in two steps at ca. 373 K [Mn(NH3)6](ClO4)2,fourmoleculesofammoniaperone
Keywords Hexaamminemanganese(II) perchlorate·
Thermal decomposition (TG/DTG/QMS)·Phase
transition·DSC·X-ray powder diffraction (XRPD)·
FT-IR
J.Hetman´czyk(&)·Ł.Hetman´czyk·A.Migdał-Mikuli·
E. Mikuli
Department of Chemical Physics, Faculty of Chemistry, Jagiellonian University, ul. Ingardena 3, 30-060 Cracow, Poland e-mail:serwonsk@chemia.uj.edu.pl
J.Hetman´czyk·Ł.Hetman´czyk
Frank Laboratory of Neutron Physics, Joint Institute for Nuclear Research, 141980 Dubna, Russian Federation
13

J.Hetman´czyketal.
1050
formula unit were freeing, compound exploded.
above
493 K
investigated
was made on aPerkin-Elmer DIAMOND 8000DSC apparatus, whereas the second run (sample B,mass=2.83 mg) was made on aMettler-Toledo 822ecalorimeter, both runs were performed in range of 123–300 K. The DSC measurements were made both during heating and cooling of the sample at constant ratesof10and20Kmin-1forsampleAand5Kmin-1forsample B. Other experimental details were the same as thosepublishedinourpreviouspaper[12].
Fourier transforms far and middle infrared (FT-FIR and FT-MIR) absorption measurements were performed usingaBruker Vertex 70vvacuum Fourier Transform spectrome- ter. The transmission spectra were collected with a reso-lutionof2cm-1andwith32scanspereachspectrum.TheFT-FIRspectra(500–50cm-1)werecollectedforsamplesuspended in Apiezon N grease and placed onpolyethylene (PE) disc. The FT-MIR spectra were collected for sample suspended in Nujol placed between KBr pellets. Temper- ature measurements were carried out usingAdvancedResearch System cryostat DE-202Aand water cooled helium compressorARS-2HWworking in a closed cycle manner. The sample was loaded at room temperature, and measurements were performed on cooling down to ca. 9 K. Thedesiredtemperaturewasmeasuredwithaccuracyof
±0.1Kandstabilizedforca.3minbeforethemeasure-mentsweretaken.TheLakeShore331Stemperaturecon-troller equipped with silicon diode sensor was used tocontrolthetemperature.Thecoolingratebetweendesiredtemperatureswasca.3Kmin-1.ThePEandKRS5win-dowswereusedinacryostatinthecaseofFT-FIRandFT-MIR measurements,respectively.
Experimental
The examined compound [Mn(NH3)6](ClO4)2was obtained from manganese(II) perchlorate hydrate (Mn(ClO4)2·xH2O)
purchasedfromSigma-Aldrich company.TheMn(ClO4)2·xH2O
complex was placed in a quartz vessel and put in a glass tube, through which dry gaseous ammonia was blown, and the tube was placed in an oven, according to the method proposed by Smith and Koch [11]. First, the tube was heated for several days up to about 400 K until the water molecule from [Mn(H2O)x](ClO4)2was lost, and hexamine complex was composed. Then, after cooling the tube to room temperature, the obtained compound was put into a desiccator for several hours in order to get rid of ammonia excess. Before the measurements were taken, the compo- sition of the compound under study was determined based on its ammonia content by titration using HCl. The average content of NH3was found to be equal to the theoretical values within the error limit of ca. 2 %.
X-ray powder diffraction (XRPD) patterns were mea-suredinacapillaryspinningadd-onusingaPANalyticalX0PertPROMPDdiffractometerwithX0Celeratordetector
operatedat40kV,30mACuKaradiation(k=1.54178A˚)
withastepsizeof0.02°.VariabletemperatureX-raypowder diffraction (VTXRD) measurements were performed in nitrogen atmosphere with the same diffractometerequipped with Oxford Cryostream system. Each powder pattern wasrecorded in the range of 3°–80°(2h).
Thermalgravimetryanalysis(TG,DTG)withsimulta-neous differential thermal analyses (SDTA) measurementswas performed using aMettler-Toledo 851eapparatus. Sampleofmass4.9826mgwasplacedina150llopencorundumcrucible.ThemeasurementsweremadeinaflowofArgon(60mLmin-1),withintemperaturerangeof300–478K.TheTGmeasurementswereperformedataconstantheatingrateof10Kmin-1.Thesimultaneousevolvedgasanalysis(SEGA)wasperformedduringthe experiments by a joined on-line quadruple mass spec-trometer (QMS) using aThermostar-Balzersapparatus. ThetemperaturewasmeasuredbyaPt–Pt/Rhthermocou-ple with an accuracy of ±0.5K.
Differential scanning calorimetry (DSC) measurements in the temperature range of 120–723 K were performed using aMettler-Toledo 822ecalorimeter. The sample of mass equals to 3.01 mg was placed in 40lLaluminium container and closed by compression. The heating rateequalsto10Kmin-1.TheDSCmeasurementsbelowroom temperature were performed using two different calorimeters. The first run (sample A, mass=8.04 mg)
Results and discussion
Crystal structure of [Mn(NH3)6](ClO4)2at 298 and 100 K
Inordertoconfirmtheidentityofthetitlecompound,theX- ray powder diffraction measurements (XRPD) at 298 and 100 K were performed. Figure1a shows the diffraction pattern collected for [Mn(NH3)6](ClO4)2at room tempera- ture. The strong reflexes were indexed in a cubic system using CRYSFIRE package and TREOR indexing program [13,14]. Analysis of the systematic absences led us to the conclusion that space group No. 225, Fm3m, can be assigned. However, in the diffraction pattern, several very weakreflexescanbealsonoticedwhichcannotbeexplained bythesuggestedcrystalsystem.Theadditionalreflexescan be easily explained by assumption that during synthesis small amount of NH4ClO4is also formed. This is not sur- prisingbecauseitiscommonlyknownthatMn2?ionisstable inslightlyacidicenvironment.Thetitledcompoundisrather
13

Thermal properties of polycrystalline [Mn(NH3)6](ClO4)2
1051
T= 298 K
(a)
observed pattern LeBail fit difference curve [Mn(NH3)6](CIO4)2
NH4CIO4
10
20
30
40
50
60
70
80
2/°
(b)
T= 100 K
Fig. 2 View of the unit cell of [Mn(NH3)6](ClO4)2at room temperature. (Color figure online)
Figure1shows a comparison of XRPD patterns reg- istered for high and low temperature phases of the dis- cussed compound. There are well-visible significant differences in the diffraction patterns registered at 298 K (high temperature phase I) and at 100 K (low temperature phase II). It indicates that crystal structure change occurs during the phase transition, which was registered by DSC at ca. 144 K (Phase transition investigations by DSC).Similar behaviour was also observed in the case of other members of hexaamminemetal(II) perchlorates,namely
10
20
30
40
2/°
50
60
70
80
Fig. 1
X-ray
powder diffraction pattern of [Mn(NH3)6](ClO4)2
for
[Ni(NH3)6](ClO4)2,
[Mg(NH3)6](ClO4)2
and
registered at 298 K (a) and 100 K (b). (Color figure online)
[Ca(NH3)6](ClO4)2[1,2,4]. Unfortunately, bad quality of the [Mn(NH3)6](ClO4)2diffraction pattern at 100 K pre- cludes determination of crystal structure of the low tem- perature phase. Attempts to index this pattern were unsuccessful.
Characteristic dependence between the values of phase
unstable, and transformation to MnO (dark grey colour of
2
thesample)isobservedwithinfewdaysevenforthesample which was kept hermetically closed. The manganese in its fouroxidationstatesisstableinaneutralenvironmentwhich isundoubtedlyformedduringprocessofammoniablowing. We have performed whole pattern fitting including both componentsofthemixtureusingLeBailmethod[15]and
FULLPROF[16]softwareinordertoobtainlatticeconstantsparameters.Thelatticeparametera=11.5729A˚was
obtained for chlorate(VII) hexaamminemanganese(II). The compound has a fluorite type structure, typical for K2PtCl6withfourmoleculesintheunitcell.Thestructureparameters are very similar to those proposed by Wyckoff [7] for other ionic hexaamminemetal(II) complexes. Figure1a shows resultsofLeBailfittingperformedfor[Mn(NH3)6](ClO4)2at RT, and Fig.2presents a view of the unit cell. The crystal structure consists of octahedral [Mn(NH3)6]2?cationsand
transition temperatureThand lattice parameterafor the
C1
compounds of the type [M(NH3)6]X2was first noticed by
Stankowski [17]. The points onThvs.adiagram for the
C1
complexeswithdifferentanionsX-(Cl-,Br-,J-,ClO-,
4
BF-,NO-,PF-)fitinseparate,characteristicforthetype
4	3	6
of the anion, areas in this diagram. Moreover, the anions
with the structure of the highest symmetry have lowerTh
C1
values than those of a lower symmetry (for exampleTh
C1
(NO-)[Th(ClO-)[Th(Cl-)).Figure3presentsTh
3
4
C1
C1
C1
a3
vs.
dependence	for	[M(NH3)6](ClO4)2,	where
M = Mg2?,
Ca2?,
Mn2?,
Fe2?,
Co2?,	andCd2?.
Ni2?
Foracomparison,Fig.3includesalsosuchdependencesfor [M(NH3)6](BF4)2and [M(NH3)6](NO3)2complexes.Fromourpointofview,thevolumeofunitcell(V=a3) isbetterparameterforsuchpresentationthanonlya.
tetrahedralClO-anions.[Mn(NH3)6](ClO)isisostructural
4
4 2
withothersimilarcomplexesofthetype[M(NH3)6](ClO4)2,whereM=Mg2?,Ca2?,Fe2?,Co2?,Ni2?andCd2?.
13
Intensity
Intensity

J.Hetman´czyketal.
1052
TG
Ni
100
Ia
240
[M(NH3)6](NO3)2
[M(NH3)6](BF4)2
[M(NH3)6](CIO4)2
Co
95
Mg
Mn
220
Ib
90
85
80
Cd
Deamination process
Decomposition with explosion
200
Ic
180
300
330
360
390
420
450
480
510
540
Ni
Co
Fe
Mg
Mn
Cd
160
0.1
0.0
–0.1
–0.2
–0.3
–0.4
–0.5
FeCd
DTG
NiCo
140
Ca
120
13.0
13.5
14.0
14.5
V/Å3× 10–2
15.0
15.5
16.0
–0.6
300
330
360
390
420
450
480	510
540
Th
versus volume of the unit cell (V=a3) dependence for
Fig. 3
C1
QMS–signal of m/e:
2?	2?
2?	2?
70
60
50
40
30
20
10
0
[M(NH3)6](ClO4)2complexes, where M = Mg , Ca , Mn , Fe ,
NH NH2NH3
Co2?,	and Cd2?. For a comparison, such dependencesfor
Ni2?
[M(NH3)6](BF4)2and [M(NH3)6](NO3)2
(Color figure online)
complexes
were
added.
scanning rate 10 K min–1sample mass 3.01 mg
10
300
330
360 390420450	480	510
Temperature/K
540
5
0
Fig. 5 TG, DTG and QMS curves for [Mn(NH ) ](ClO )
registered
36	42
Deaminationprocess
Decompositionwith explosion
atheatingrateof10Kmin-1inthetemperaturerangeof300–478K.(Color figure online)
Phase transition in solid state
–5
–10
all NH3ligands. The process of deammination undergoes according to the following reactions:
–15
IaMnðNH3Þ6ðClO4Þ2!MnðNH3Þ4ðClO4Þ2þ2NH3
–20
NH4CIO4
ð1Þ
–25
IbMnðNHÞ ð

200
300
400
500
600	700
800
900
ClOÞ!MnðNHÞðClOÞþ2NH
Temperature/K
3
4
3
4
3
4
2
2
2
ð2Þ
ð3Þ
Fig. 4 DSC curve for [Mn(NH ) ](ClO ) registered at heating rate
36	42

-1
of 10Kmin	in the temperature range of 120–900 K. Lower curve (green line) corresponds to pure NH4ClO4. (Color figureonline)
IcMnðNH3Þ2ðClO4Þ2
!MnðNHÞðClOÞþð2-xÞNH

3
4
3
x
2
IIMnðNHÞðClO4Þ2-!

540 K
decomposition with explosion
3
x
Thermal behaviour of the title compound (recognition by DSC, TG, DTG, QMS)
ð4Þ
Endothermic peak registered in DSC curve at 519 K is connected with the phase transition in solid state of NH4-ClO4, which in small amount is also formed during the synthesis of [Mn(NH3)6](ClO4)2. Above 538 K, we observed the decomposition with explosion of manga- nese(II) perchlorate.
Figure5presents TG, DTG and QMS curvesrecorded for [Mn(NH3)6](ClO4)2at a constant heating rate of10Kmin-1inthetemperaturerangeof300–478K(abovethis temperature sample explodes). During theTG
Figure4showstheDSCresultsobtainedinthetemperaturerangeof123–723Kwiththescanningrateof10Kmin-1for[Mn(NH3)6](ClO4)2sampleclosedinaluminiumvessel. This measurement was performed before TG analysis in order to check the stability of the compound and toqual- itativecomparisonoftheseresultswiththermalanalysis.
Three endothermic peaks clearly visible in DSC curve
for [Mn(NH ) ](ClO ) in the temperature range of 400–
36	42
515 K (Fig.4) are associated with the liberation of almost
13
Heat flow/mW
Tc/K
Endo
m T–1/mg K–1
m/%
Ion current/nA

Thermal properties of polycrystalline [Mn(NH3)6](ClO4)2
1053
Table 1 Parameters of [Mn(NH3)6](ClO4)2thermal analysis
Sample mass/mg
Stage number
Temperature range/K
Mass loss at the stage/%
Mass after decomposition/%
Calculated values/%
Products of the decomposition
4.9826
Ia Ib Ic
II
300–398
398–448
448–478
Above 540
9.4
9.8
1.1
9.6
9.6
2 NH3
2 NH3NH3
Explosion
experiment, the QMS spectrum of masses was followed fromm/e=1–100, however, for reasons of graphic read- ability, only the masses ofm/e=15, 16 and 17—repre- senting NH, NH2and NH3are shown. The TG, DTG andQMS curves indicate that the deammination undergoes in thethreesteps (Ia, Ib and Ic). Statistically, at step Ia, 2 molecules of ammonia per one formula unit are freeing, the next 2 molecules of ammonia are freeing at step Ib and the rest in step Ic. The temperatures, percentage mass of losses and the products of the decomposition of [Mn(NH3)6] (ClO4)2at particular stages are presented in Table1. The temperature ranges of sample transformation were taken from the DSC measurements. They are shifted with respect to TG measurements towards a little bit higher tempera- tures. The reason is slightly different conditions during measurements. The DSC was performed for sample closed in alumina vessel with micro-hole, whereas the TG investigations were performed in open crucible.
The results obtained in this paper differ slightly from those presented so far in the literature. The process of deammination is also different. From our study, it is clearly
deamminated manganese(II)
and
nickel(II) compounds,
respectively, decomposed. In case of [Mn(NH3)](NO3)2, deammination takes place at even lower temperature (ca. 450 K).
Phase transition investigations by DSC
Figure6presents the temperature dependence of the heat flow obtained for the title compound on heating (upper curve) and on cooling (down curve) for sample B of[Mn(NH3)6](ClO4)2attherateof5Kmin-1.Onedistinctanomaly on each of these two DSC curves at
Th
= 143.6 andTc
= 137.8 K (where indexes h and
Cpeak
Cpeak
c denote heating and cooling of the sample, respectively). The pure NH4ClO4does not exhibit any phase transition in that region (see for comparison in Fig.4). These phase transition temperatures were calculated by extrapolating
the corresponding dependencies ofTh
andTc
values
Cpeak
Cpeak
versus the scanning rate dependences, registered atscan-ningratesofheatingandcoolingthesample:5,10and20Kmin-1,tothescanningratevalueequalto0Kmin-1.Themeanvalueofthephasetransitiontem-
visible that [Mn(NH ) ](ClO ) firstly loses two molecules
36	42
ofammonia,andnexttwomoleculesarefreeing(stepIaand Ib).Furtherheatingcausesthatnotcompletelydeamminated manganese(II)perchloratedecomposeswithexplosionatca. 540 K. The temperature of explodes discovered by us is ca. 50 K higher than given in [10]. The explosion of the com- pounds containing perchlorate anion during the thermal decomposition is a common feature of these complexes: [Ca(NH3)6](ClO4)2and [Sr(OS(CH3)2)6](ClO4)2[18,19].
Comparing the thermal decomposition processes of [Mn(NH3)6](ClO4)2and [Ca(NH3)6](ClO4)2[18], regis-
tered at a constant heating rate in a flow of Argon, we noticed that they proceed in different ways. The main difference is in the temperature range in which all mole- cules of ammonia are freeing. It can be seen that in case of [Mn(NH3)6](ClO4)2, the particular NH3ligands are liber- ated in a much lower temperature (300–515 K) than theNH3in [Ca(NH3)6](ClO4)2(341–601 K). The temperature of explosion discovered by us for [Mn(NH3)6](ClO4)2is ca. 150 K lower than observed for [Ca(H2O)4](ClO4)2(above 700 K). Thermal decomposition of the investigated com- pound is similar to [Mn(NH3)](NO3)2[20] and [Ni(NH3)](NO3)2[21]. In both cases, not completely
Th
perature	is
=143.5K	(on	heating)	and	at
C1
Tc
=137.6 K (on cooling) with the estimated entropy
C1
changeDS=21.6±0.3Jmol-1K-1.Thelargetransi-tion entropy change indicates considerable configurationaldisorder in the high temperature phase (so called ODIC crystals [22] ). The presence of 5.9 K hysteresis of the
phase transition temperature at and sharpness of the anomaly attest that the detected phase transition is of the first-order type. Thus, the title compound has two solid phases in the temperature range of 123–300 K: high tem- perature (phase I) and low temperature phases (phase II). The thermodynamic parameters of the detected phase
TC1
transition obtained during heating are presented in Table2. The values of entropy change accompanying these phase transitions suggest also theirs ‘order–disorder’ mechanism.
Vibrational motions and phase transition
Vibrational FT-IR spectra for [Mn(NH3)6](ClO4)2were measured as a function of temperature. The list of the band
13

J.Hetman´czyketal.
1054
2.5
Table 3 The list of band positions of the infrared spectra of [Mn(NH3)6](ClO4)2at room temperature (vwvery weak,wweak,shshoulder,mmedium,ststrong,vstvery strong,brbroad)
scanning rate 5 K min–1Phase transition
sample mass 2.83 mg
in solid state
Th
= 143.6 K
2.0
c
Frequenciesofvibrations/cm-1
Assignments
heating
IR at 295 K
IR at 9 K
1.5
3385 m
3293 m
3388 st
3295 m
3265 m
3200 sh
1616 vw
1605 m
1595 vw
1300 w
1197 m
1172 vw
1161 w
1086 vst
935 vw
915 vw
889 vw
767 vw
627 m
594 m
460 vw
421 br
296 m
184 st
76 st
68 st
60 vw
mas(NH)F1ums(NH)F1ums(NH)F1ums(NH)F1udas(HNH)F1udas(HNH)F1udas(HNH)F1uds(HNH)A1gds(HNH)F1uds(HNH)F1uds(HNH)F1umas(ClO)F2ms(ClO)A12d(OClO)E?A1
2d(OClO)E?A1
1.0
cooling
3189 sh
0.5
1609 m
Tc
= 137.8 K
c
0.0
120 140 160 180
200 220 240
260 280
300 320
1303 w
1205 m
Temperature/K
Fig. 6 DSC curve obtained for [Mn(NH ) ](ClO ) on heating
36	42
(upper curve) and cooling (lower curve) with a scanning rate of5Kmin-1.(Colorfigureonline)
1092 vst
937 vw
916 vw
894 vw
768 vw
626 m
591 m
Table 2 Thermodynamic parameters of the phase [Mn(NH3)6](ClO4)2
transitions of
d(OClO)F
d
2
Thermodynamicsparameters
TC/K
DH±DdH/
kJmol-1
DS±DdS/
Jmol-1K-1
qr(NH3)F1u
d(OClO)E
d
417 br
283 m
179 st
76 st
70 v
60 vw
ms(Mn–N)A1gmas(Mn–N)F1udas(NMnN)F1umL(lattice)EgmL(lattice)EgmL(lattice)Eg
Heating
Cooling
143.6±0.1
137.8±0.1
3.1±0.2
3.0±0.3
21.6±0.3
21.8±0.3
positions,
their
relative intensities and tentative assign-
ments are listed in Table3. The assignments of these vibrations were proposed by comparing their frequencies with the literature data collected for titled compounds and similar ionic perchlorate amminemetal(II) complexes [10,23–27]. All characteristic bands frequencies of the internal vibrations were found. These assignments proved that the composition and structure of the investigated compound are correct. Detailed description and analysis of vibrational modescanbefoundinMikulietal.[20].
Figure7shows the FT-FIR spectra of [Mn(NH3)6](ClO4)2withinthewavenumberrangeof500–50cm-1registered during the cooling of the sample from 290 to 9 K. The spectrum at the lowest temperature containssevenbands.Threeofthemat60,68and76cm-1areassociated with themLlattice vibration modes. Next threebandsat184,296and421cm-1areassociatedwiththeinternal vibrations of [Mn(NH3)6]2?ion of the modes:das(NMnN),mas(Mn–N) andms(Mn–N), respectively.Some interesting changes can be noticed for the band at288cm-1(RTtemperature)associatedwithstretchingmodemas(Mn–N)F1u.Apartfromnarrowingofthisband,
the shifting towards higher wavenumbers is visible during the cooling of the sample, especially in the region of thephasetransition.Thelastbandat460cm-1isconnected
withtheClO-anionnormalmoded(OClO)E.
4
d
Thetemperature-dependentFT-MIRspectrawerealsorecordedduringacoolingofthesample.Figure8shows exemplarily the spectra in the wavenumber ranges:4000–3040,1840–1500and1300–500cm-1,atselectedtemperaturesofmeasurement.Someevidentchangesinthe spectraatthetemperatureregionofthephasetransitioncan benoticed.Namely,apartfromofthenarrowing,thesplit- tingofsomebandscanbeseenbelowthephasetransition.AsonecanseeinFig.8,newbandsstarttoappearinthespectraoncoolingjustafterthephasetransitiontemperature(atca.130K)inthewavenumberrange(1200–1150cm-1),connectedwiththeds(HNH)F1umode.Thus,accordingto theinfraredspectroscopypointofview,achangeofthepointsymmetrytakesplaceatthephasetransition.
13
Heat flow/mW
Endo

Thermal properties of polycrystalline [Mn(NH3)6](ClO4)2
1055
Conclusions
s(Mn–N)
The results obtained in this work and their comparison with the literature data led us to the following conclusions:
X-ray powder diffraction (XRPD) measurement at room
temperature indicated that [Mn(NH3)6](ClO4)2has astructureofcubicsymmetry(spacegroup:Fm3-m,No.225)with four molecules in the unit cell and lattice parameter
a=11.5729A˚.Thecrystalstructureconsistsofoctahedral
295 K
260 K
240 K
210 K
[Mn(NH3)6]2?cationsandtetrahedralClO-anions.
4
[Mn(NH3)6](ClO4)2is isostructural with the [M(NH3)6] (ClO4)2compounds that are studied earlier by us. XRPD pattern registered at 298 K (high temperature phase I) is different than that obtained at 100 K (low temperature phase II). Changes observed in diffraction patterns of [Mn(NH3)6](ClO4)2suggest that the phase transition atTc
180 K
150 K
140 K
c
130 K

100 K
Tc
C1
is associated with a change of the crystal structure.
70 K
50 K
9 K
Differential scanning calorimetry (DSC) measurements of [Mn(NH3)6](ClO4)2performed in the temperature range of 123–295 K allowedto detect onesolid–solid phasetransition. The temperature of this phase transition amount
500 450 400 350 300 250 200 150 100
Wavenumber/cm–1
toTh=143.5 K (on heating) and atTc=137.6 K (on
C1
C1
Fig. 7 Selected FT–FIR spectra in the wavenumber
range
of
cooling). Thermal hysteresis of the phase transition tem- perature (DTC&5.9 K) and entropy change value(DS=21.6Jmol-1K-1)connectedwiththisphasetran-sitionindicatethatitisofafirst-ordertype,suggestthatit is of ‘order–disorder’mechanism.
In this work, it has been determined that for [Mn(NH3)6](ClO4)2, the values of phase transition tempera- ture and lattice parameteravery well fit the graph of vs.aoutlined earlier for the family of [M(NH3)6](ClO4)2compounds.
The investigated sample is unstable in time and tem- perature. Thermal gravimetry analysis (TG) and DSC measurement informed us that deammination process begins only just at ca. 398 K and above 538 K the decomposition with explosion of manganese(II) perchlo- rate was observed.
Appearing of the two new bands (splitting ofds(HNH)F1umode) in the FT-MIR spectra at the vicinity of1,200cm-1,suggeststhatthephasetransitioncrystalstructure undergoes achange.
500–50cm-1atdifferenttemperaturesregisteredatcoolingofthe
[Mn(NH3)6](ClO4)2. Phase transition temperature registered by DSC also at cooling is indicated byarrow. (Color figure online)
* *
(N–H)
as
s(NH3)
as(NH3)
*
295 K
260 K
240 K
210 K
180 K
150 K
140 Kc
Tc
130 K
100 K
70 K
50 K
9 K
39003600 3300
1800
1600 140012001000
600
800
Wavenumber/cm–1
Fig. 8 Middle infrared spectra in the wavenumber4000–3040,1840–1500and1300–500cm-1atdifferent
ranges: selected
temperatures (at cooling of the [Mn(NH3)6](ClO4)2sample in Nujol). Phase transition temperature registered by DSC also at cooling is indicated byarrow. (Color figure online)
Acknowledgements The infrared absorption (FT-MIR) researches were carried out with the equipment purchased thanks to the financial support of the European Regional Development Fund in the frame- work of the Polish Innovation Economy Operational Program (con- tract no. POIG.02.01.00-12-023/08).
Thenarrowingofdas(HNH)F1u(1628cm-1)and
mas
Open Access This article is distributed under the terms of the Creative Commons Attribution License which permits any use, dis- tribution, and reproduction in any medium, provided the original author(s) and the sourceare credited.
(NH)F	(3385cm-1),bandswithtemperaturedecreasing,
1u
indicates slowing of their fast reorientational motions in the vicinity of phase transition.
13
Absorbance
Absorbance

J.Hetman´czyketal.
1056
References
1. Werner PE, Eriksson L, Westdahl M. TREOR, a semi-exhaustivetrial-and-error powder indexing program for all symmetries. J Appl Crystallogr.1985;18:367–70.
2. Le Bail A, Duroy H, Fourquet JL. Ab-initio structure determi-nation of LiSbWO6by X-ray powder diffraction. Mater Res Bull. 1988;23:447–52.
3. Rodriguez-CarvajalJ.Recent advancesinmagnetic structure deter-minationbyneutronpowderdiffraction.Phys B.1993;192:55–69.
4. StankowskiJ. Structure phase transitions in Me(NH3)6X2. Mater Sci II.1976;11(3):57–62.
5. Migdał-MikuliA,Hetman´czykJ.Thermalbehaviorof[Ca(H2-O)4](ClO4)2and [Ca(NH3)6](ClO4)2. J Thermal Anal Calorim. 2008;91:529–34.
6. Migdał-Mikuli A, Szostak E, Paweł Bernard P. Thermalanalysis,
1. Migdał-Mikuli Investigation
A, Mikuli E, Rachwalska M, Hodorowicz S. of the phase situation inpolycrystalline
[Mg(NH3)6](ClO4)2by adiabatic calorimetry and X-ray diffrac- tion methods. Phys Status Solidi A. 1978;47:57–64.
1. Hodorowicz S, Ciechanowicz-Rutkowska M, Janik JM, Janik JA. The X-ray powder investigation of phase transitions in [Ni(NH3)6](ClO4)2. Phys Status Solidi.1977;43:53–7.
2. Rachwalska M, Janik JM, Janik JA, Pytasz G, Waluga T.Specific heat of solid [Ni(NH3)6](ClO4)2in the temperature range from 115to300K.PhysStatusSolidiA.1975;30:K81–2.
3. Hetman´czykJ,Migdał-MikuliA,Hetman´czykŁ.Phasetransitionand molecular motions in [Ca(NH3)6](ClO4)2. Ann Polish ChemSoc. 2007;358–61. ISBN978-83-922424-7-5.
4. Hetman´czykJ,Hetman´czykŁ,Migdał-MikuliA,MikuliE,
Natkaniec I. Phase transition in [Ca(NH3)6](ClO4)2studied byneutron scattering methods and far infrared spectroscopy. J AlloyCompd. 2011;509:6545–50.
1. Migdał-MikuliA,MikuliE,Wro´belS,Hetman´czykŁ.DSCInvestigationsofthephasetransitionsof[M(NH3)6](ClO4)2and[M(NH3)6](BF4)2, where M = Co and Cd. Z. Naturforsch. 1999;54:590–4.
2. WyckoffRWG. Crystal Structures. 2nd ed., vol. 3. IntersciencePublishers, New York;1965.
3. Janik JM, Janik JA, Migdał-Mikuli A, Mikuli E, Otnes K. Neu- tron quasielastic scattering results for [Me(NH3)6](XY4)2, [Me(NH3)6](XY3)2and [Me(NH3)6](XY2)2compounds, com-pared with the calorimetric and Raman line width data—a new analysis. Phys B.1991;168:45–52.
4. Dynowska E, Stankowski J. X-ray study on the structural phasetransition in nickel hexammine perchlorate. Phys Status Solidi A. 1979;52:381–6.
5. PatilKC, Pai Verneker VR, Jain SR. Metal perchlorate ammines: thermal and infrared studies. Thermochim Acta.1976;15:257–60.
6. Smith GF, Koch EG. Darstellung und Eigenschaften der Perchl-oratamminederErdalkalimetalle.ZAnorgChem.1935;223:17–27.
7. MikuliE,Migdał-MikuliA,Wro´belS.Phasetransitionsincrystalline [Me(H2O)6](BF4)2. Part I (Me=Mn, Fe Co, Ni and Zn). Z Naturforsch.1999;54:225–8.
8. Shirley R. The CRYSFIRE system for automatic powder index- ing:user’smanual.Guildford,Surrey:TheLatticePress;2000.
phase
transitions
and
molecular
reorientations
in
[Sr(OS(CH3)2)6](ClO4)2.JThermalAnalCalorim.2014;115:443–9.
1. MikuliE,Liszka-SkoczylasM,Hetman´czykJ,SzklarzewiczJ.Thermal properties, phase transitions, vibrational and reorienta- tional dynamics of [Mn(NH3)6](NO3)2. J Thermal Anal Calorim. 2010;102:889–97.
2. Mikuli E, Migdał-Mikuli A, Majda D. Thermal decomposition of polycrystalline [Ni(NH3)6](NO3)2. J Thermal Anal Calorim. 2013;112:1191–8.
3. Lovesey SW. Dynamics of solids and liquids by neutron scat- tering. In: Springer T, editor. Topics in current physics, vol. 3. Berlin: Springer-Verlag;1977.
4. Nakamoto K. Infrared and Raman spectra of inorganic and coordination compounds. 5th ed. New York: Wiley-Interscience Publication;1997.
5. Migdał-MikuliA,MikuliE,Baran´skaM,Hetman´czykŁ.
Vibrational spectrum and molecular structure of [Cu(NH3)5](- ClO4)2. Chem Phys Lett. 2003;381:329–34.
1. Druz_bicki K, Mikuli E. Experimental (FT-IR and FT-RS) and theoretical (DFT) studies of molecular structure and internal modes of [Mn(NH3)6](NO3)2. Spectrochim Acta A. 2010;77:402–10.
2. Janik JM. editor. Fizyka chemiczna. PWN, Warszawa; 1989 (in polish).
3. Janik JA, Janik JM, Migdał-Mikuli A, Mikuli E, Rachwalska M, Stanek T, Otnes K, Fimland BO, Svare I. Calorimetry, proton magnetic resonance and quasielastic neutron scattering studies of [Mg(NH3)6](NO3)2. Phys B.1983;122:315–20.
13