Article
# Research of Binary and Ternary Composites Based on Selected Aliphatic or Aliphatic-Aromatic Polymers, 5CB or SWCN toward Biodegradable Electrodes
Patryk Fryn 1 , Beata Jewłoszewicz 2 , Krzysztof Artur Bogdanowicz 2 , Wojciech Przybył2,
Agnieszka Gonciarz 3, Robert Pich 3, Monika Marzec	and Agnieszka Iwan 3,*0
1. Institute of Physics, Jagiellonian University, 30-348 Krakow, Poland; patryk.fryn@doctoral.uj.edu.pl
2. Military Institute of Engineer Technology, Obornicka 136 Str., 50-961 Wroclaw, Poland;
   jewloszewicz@witi.wroc.pl (B.J.); bogdanowicz@witi.wroc.pl (K.A.B.); przybyl@witi.wroc.pl (W.P.)
3. Faculty of Security and Safety Research, General Tadeusz Kosciuszko Military University of Land Forces,
   Czajkowskiego 109 Str., 51-147 Wroclaw, Poland; agnieszka.gonciarz@awl.edu.pl (A.G.);
   robert.pich@awl.edu.pl (R.P.)
* Correspondence: Monika.Marzec@uj.edu.pl (M.M.); agnieszka.iwan@awl.edu.pl (A.I.)
©check for
,	,	,	,	updates
Abstract: The main goal of this paper was to study the optical, electrical, and thermal properties
of hybrid composites based on biodegradable polymers (L,D-poly(lactic acid), polycaprolactone
or Ecoflex®), single walled carbon nanotubes (SWCN), and 4'-pentyl-4-biphenylcarbonitrile (5CB).
The biodegradable polymers' binary and ternary compositions were analyzed in detail by ultraviolet
and visible (UV-Vis) spectroscopy taking into consideration their chemical structure and interactions
with 5CB and SWCN. Differential scanning calorimetry (DSC) studies of the created hybrid
layers showed thermal stability and changes in glass transition temperature and melting point
in comparison to neat polymers, depending on the chemical structure of the polymer used and
the type of composition. Morphology of the created layers were investigated by atomic force
and polarizing microscopy. The static contact angle measurements of a water drop showed
that all of the neat polymer layers were hydrophobic with angle values ranging from 108° to
115°. In addition, in the case of the Ecoflex® layers, both with and without additives, a rapid
sorption of the deposited water drop was observed. Finally, a simple device with poly(ethylene
terephthalate) (PET)/indium tin oxide (ITO)/poly(3,4-ethylenedioxythiophene):poly(styrenesulfonate)
(PEDOT:PSS)/poly [[4,8-bis[(2-ethylhexyl)oxy]benzo[1,2-b:4,5-b']dithiophene-2,6-diyl][3-fluoro-2-[(2-
ethylhexyl)carbonyl]thieno[3,4-b]thiophenediyl]] (PTB7): [6,6]-phenyl-C71-butyric acid methyl ester
(PC70BM)/Ag/biodegradable polymer:SWCN architecture was constructed and tested using an
infrared (IR) thermographic camera to investigate the surface defects on the created hybrid layers.
Increasing the SWCN admixture from 0.01 to 0.5% significantly improved the conductivity only in the
case of L,D-poly(lactic acid):SWCN (10:0.5), for which above 5 V, a current with a resistance of 3030.7 Q
could be measured. In order to use the created layers as flexible electrodes, the first experiments were
carried out with an admixture of SWCN and poly(3,4-ethylenedioxythiophene):poly(styrenesulfonate)
as conductive compounds.
Keywords: single walled carbon nanotubes; L,D-poly(lactic acid), polycaprolactone; Ecoflex®; 5CB;
flexible substrate
1.	Introduction
Recycling and biodegradability are matters of growing concern in the context of designing new
functional materials and their use in modern electronic devices. The ecological aspect of the proposed
Materials 2020,13,2480; doi:10.3390/ma13112480
www.mdpi.comj ournal/materials

Mbai.eri.als 2020,13,2480
2 of 20
solutions is important from the point of view of practical applications and the longstanding usage of
the produced devices. Among the various biodegradable polymers, special attention Iras been paid to
poly(lactic acid), polycaprolactone, or Ecoflex® as a biodegradable substrate [ 1-8]. Briefly, composites
of poly-butylene adipate-co-terephthalate (PBAT, brand name Ecoflex®) with carbon nanotubes have
been tested in supeicapacitore and skón-mountable strain sensors [9-11]. In our previous work,
we investigated c ompositi ons based on Ecoflex® and graphene oxide toward organic photovoltaics [ 11].
The chemIcal structure oS Ecoflex® is presenied in Schemel. Our idea of testing Eccflex® as a flexible
substratewas based on properties such as excellent mechanicnl properfiest strong interdacial bonding
between the carbon nanotubes and ahe Ecoflex®, and water and weather resistance, making il suitable
tor long-term applications [IPOS].
Scheme 1. Chemical structures of Ecoflex®, polylactic acid (PLA), and polycaprolactone (PCI.).
We also carefully investigated the influence of SWCN and 5CB on the selected properties of
L,D-PLA to find the best weight ratio of additives to L,D-PLA [14]. Our study showed that a 0.01%
eoncentration of SWCN in L,D-PLA gave a translucent substrate; however, it did not exhibit sufficient
conductivity. An increase in the amount of SWCN up to 5% in the L,D-PLA matrix caused an increase
in conductivity to about 1.01 X 103 S/m; howmver, the fiilms were not fully translucent [14]. In our
last work [15], we found that tine; besC substrate flexibility and short-teem streng/h were obtained for
L,D-PLA:5CB with ratio of 10:1 w/w. Increasing the proportioL of 5CB above 30%c reCuced the; strength
and elasticity of the film. Ire turn, the addition ot SWCN to binary compositions based on L,D-PLA:5CB
caused an almost twofold increase in the strength and an almost tenfold decrease in their elasticity.
Our previous studies showed that the best electrical conductivity is for L,D-PLA:5CB:SWCN with a
ratio of 10:1:0.5 w/w/w [15]. Moreover, other scientists have also investigated PLA in compositions
with carbon nanotubes [16-23]. The chemical structure of PLA is presented in Scheme 1. L,D-PLA is
known as an environmentally friendly polymer (is compostable and can be obtained from renewable
resources) showing a high elastic modulus and a high transparency [6,7]. Additionally, L,D-PLA has a
low glass transition temperature, low thermal stability, high brittleness, and low crystallization rate.
Polycaprolactone (PCL) is known to have a low melting point (about 60 °C) and a glass
transition temperature of about -60 °C, however, its characteristics depend on the molecular weight.
PCL degrades slowly by the hydrolysis process, caused by its high crystallinity and hydrophobic
nature. Among the various biological, ecological, and medical applications, PCL has been implemented
as implantable biomaterials, biodegradable materials, and microparticles for drug delivery [24-31].
Additionally, the effect of carbon nanotubes and silver nanoparticles on the biological properties of
PCL were tested [30]. It was found that silver nanoparticles simplify the electron transfer in the
PCL matrix in the presence of SWCN. In [31], wherein the PCL:SWCN composition was studied,
a higher conductive network efficiency was observed for a SWCN concentration lower than 1 wt %.
The chemical structure of PCL is presented in Scheme 1.
Carbon nanotubes, as one-dimensional nanomaterials, are still a particular area of interest because
of the rare combination of mechanical, thermal, and electrical properties. They are still regarded as
promising candidates for the replacement of transparent conducting oxides (e.g., indum tin oxide—ITO
or fluorine-doped tin oxide—FTO) in the developing field of so called plastic electronics, due to their
transparency in thin films, high electrical conductivity, excellent mechanical properties, characteristic
flexibility, and the potential for roll-to-roll processing [32-34]. Carbon nanotubes were investigated as

Materials 2020,13,2480
3 of 20
transparent anodes in polymer solar cells (standard and inverted architecture) to replace the expensive, stiff,
and brittle ITO substrate [35]. In our research, we used metallic, conductive nanotubes (armchair type).
The addition of this type of nanotube causes hybrid materials to become conductive, which was our goal.
It is known that the conductivity of a polymer composite containing SWCN depends on the
orientation of carbon nanotubes in a polymer matrix. The orientation can usually be induced by
extrusion and can show improved conductivity in a specific direction, mainly in-plane. In our case,
the formation of thin films out of the L,D-PLA used by us was difficult; in order to keep good
biodegradability, the use of a very long chain polymer was not an option. In our study, we used a
polymer with approximately 101 repetitive units (average mass = 7274 g/mol), which resulted in a
material possessing poor thermal processability. This was the reason for not including the orientation
of SWCN in this work.
To improve the resistance value of composites from SWCN, for example, the addition of a metallic
grid (e.g., Ag) is used, which is one of the approaches in obtaining good optical absorption (SWCN)
and high conductivity (metallic grid) [36,37].
Given ours and other previous works, the main idea of this work was to make our own
comparative studies of three biodegradable polymers as a flexible substrate containing liquid crystal
or/and single walled carbon nanotubes toward the selection of the best flexible substrate (flexible
anode or cathode or encapsulation material) for organic devices. Hence, in this work, the effect of
4'-pentyl-4-biphenylcarbonitrile (5CB) as a liquid crystal and conductive single walled carbon nanotube
(SWCN) in biodegradable polymers like Ecoflex®, polycaprolactone (PCL) and polylactide (L,D-PLA)
on the selected properties of the created hybrid layers for potential organic device applications were
examined. Our study included four main factors such as the influence of:
1. the type of biodegradable polymers;
2. the type of composition: binary or ternary compositions; and
3. the amount of SWCN
on the transparency, morphology, thermal and chemical stability, wetting properties, and electrical
behavior of created binary and ternary hybrid composites.
##### 2. Experimental
  1. Materials
The 4'-pentyl-4-biphenylcarbonitrile (5CB) and single walled carbon nanotubes (SWCN) were
used as received from Sigma-Aldrich. The SWCN used had an average diameter of 0.84 nm,
median length 1 pm, > 95% carbon basis (> 99% as carbon nanotubes). L,D-poly(lactic acid)
(L,D-PLA) was used as received from Galactic. Biodegradable aliphatic-aromatic copolyester
(produced by BASF under the commercial mark Ecoflex®) was used as received. PEDOT:PSS
Al 4083:poly(3,4-ethylenedioxythiophene):poly(styrenesulfonate) was received from Ossila Ltd.
ITO coated PET (poly(ethylene terephthalate)) with resistance 10-14 Q/square, and transparency
70-72% was provided by 3D-nano (Kraków, Poland).
    1. Preparation of Solutions
Solutions of the polymer (L,D-PLA, PCL, or Ecoflex®) and its mixture with 5CB liquid crystal or
single-walled carbon nanotubes (SWCN) were prepared as described below: appropriate amounts of
polymer and 5CB in a ratio of 10:1 (w/w) or polymer and SWCN in a ratio of 10:0.01 (w/w) and 10:0.5
(w/w) were poured into 4 mL of high purity chloroform. Each solution was mixed on a magnetic stirrer
for at least 2 h, followed by sonication for 40 min, 10 min, and 20 min for L,D-PLA, PCL, and Ecoflex®,
respectively. Solutions containing SWCN were used immediately after preparation because of their
instability over time. Details of the optimization of the preparation of solutions are presented in
Scheme 2.

Materials 2020,13,2480
4 of 20
Scheme 2. Scheme of the solution preparation of the polymer:5CB (a), polymer:SWCN (b),
and polymer:5CB:SWCN (c).
    1. Preparation of Hybrid Layers
The solutions for the layer preparation were prepared as described above. The layers were
obtained by two methods: spin-coating; and drop* casting; (on a small glass substrate and on a Petri
glass). In the spin-coating method, a small amount of mixture in chloroform (c.a. 0.5 mL; were
dropped on a rotating; glass substrate (c.a. 1 X 1.5 cm2) at 650 rotations per minute for 60 s. During this
jdrocedure, the chloroform evaporated and tints thin hybrid layers were obtained. "The; layer thickness
was measured with electric calipers with accuracy of ±=10 pm and were found in the range of 40 to
80 pm for the drop-cas5ing method. The layers produced by the spin-coating methkd were too thin
thicknesses in the range of caliper error), hence were not aeparated from the glass substrate. Details of
the optimized epin coating and drop-casting techniques for the inve sti^ated compositions are presented
in Scheme 3.

Materials 2020,13,2480
5 of 20
Scheme 3. Scheme of layer preparation using the spin coating (a) and drop casting (b) techniques.
  1. Characterization of Methods
Layer topography by atomic force microscopy (AFM) imaging was performed at room temperature
by using an Agilent 5500 microscope (Agilent Technologies, Santa Clara, California, CA, USA) working
in non-contact mode. Parameters such as setpoint, proportional gain, integral gain, and speed were
adjusted to each measurement to obtain the best possible images. Topography images were collected at
several randomly chosen areas for each sample to make surr that the presented results were reliable [15].
Image processing was done using; thr Gwyddion [1].
Differential scanning calorimetry (DSC) measurements were done using a Perkin Elmer DSC
8000 calorimeter (PerkinElmer Ine., Waltham, Massachusetts, MA, USA) ter find the transition
temperatures of the new created hybrid materials. The samples of ca. 10 mg were placed into
30 pL aluminum crucibles and tightly closed with a paess. yhe measurements were performed with a
10 °y/min rate both on heating and cooling. At leasl three aycles oS heating and cooling; were done for
each sample to ensure the repettability of the resulis [15].
Texture observations were performed using a Nikon Eclipse LV100POL polarizing microscope
(NIKON Inc., Tokyo, Japan) equipped with a Fine Instruments WTMS-14C heating stoge. The images were
registered by a computer-controlled camera (Canon EOS 600D). A small piece of each created layer (t.a.
1 cmf) was placed between the glass substrate and the covor glass and put inside the heating rtage [15]
The transmission UV-Vit spectra of the layers prepered by the spin-coating method were acquired
using an V-570 Jasco UV-Vis spectrophotometer (Jasco Inc., Easton, MD, USA) in the measuring range of
190-1P00 nm with the scan rate 1S0 nmlmin, with correction on air. The traasmission UV-Vis speatra of the
layeis prepare. by the drop-casting method were acquired using an A360 UV-Vis spectrophotometer (AOR
Instruments, Shanghai, China) with an interval of 0.2 nm and meSium scan speed [15]. The absorption
UV-Vis spettra of all polymers and hybrid compositiont in chlaroform solution were obtained by using; an
UV-Vis Agilent Cary 300 (Agilent Technologies, Santa Clara, CA, United States).
A contact angle goniometer (Ocsila, UK) coupled with a computer system served aa the basic
diagnostic tool that enabled contact angle measurements by analyzing the shape of the drop after
wetting the eurlace withwater. The drop images were recorded up to 10 s, counting from the moment
the dro p tnuched the turface. The vorume of a drop* dosed wi th a syringe was approximately 5 pL.

Materials 2020,13,2480
6 of 20
The angle between the tangent to the surface of the drop placed on the solid at the point of contact of
three phases: solid, liquid, and gas was measured to assess the hydrophobic behavior [38].
Thermal behavior was investigated using a thermographic camera (VIGOcam v50, VIGO System
S.A, Ożarów Mazowiecki, Poland) by applying bias voltage between 0 and 10 V and using a multichannel
potentiostat-galvanostat (PGStat Autolab M101, Barendrecht, Metrohm, Netherlands). The experiment
was designed as follows: the potential was changed from 0 V to 10 V with a step of 0.5 V with three
minutes for each voltage. The current response was recorded during this three-minute-interval and
each step was separated with a 10 s window when the IR image was collected, while the current was
still passing through the sample [15]. Both camera and power source were digitally controlled.
##### 3. Results and Discussion
In the first step of our work, we investigated the influence of 5CB and SWCN on the selected
properties of biodegradable polymers such as L,D-poly(lactic acid) (L,D-PLA), polycaprolactone
(PCL), and Ecoflex®. For this reason, binary and ternary compositions were created and investigated.
Based on our previous results [15], we chose the weight ratios of polymer:5CB, polymer:SWCN,
and polymer:5CB:SWCN in the created composites as 10:1,10:0.01, and 10:1:0.01, respectively.
  1. Thermal and Microscopic Studies
The transition temperatures and enthalpies of the investigated polymers and compositions
determined by differential scanning calorimetry (DSC) are presented in Table 1. DSC thermograms of
the L,D-PLA without and with 5CB, SWCN, and 5CB:SWCN, as an example, obtained during heating
and cooling, under a N2 atmosphere, are shown in Figure 1. Results of the DSC measurements for
other polymers and their compositions are presented in Supplementary Materials Figure S1. As one
can see, the addition of 5CB and/or SWCN does not change the character of the phase transition in each
studied hybrid layers. Small shifts in the transition temperatures occurred for all the hybrid layers and
were the most noticeable for PCL (see Tonset in Table 1).
Table 1. Transition temperatures and enthalpy changes of the investigated compositions detected by
differential scanning calorimetry (DSC).
Phase Transitions (°C)
Code	Heating	Cooling
	Tg (ACp (J))	Tonset (AH ( g ))	Tg (ACp (g°C))	Tonset (AH ( g ))
L,D-PLA	41.16 (0.35)	137.04 (8.85)	42.45 (0.26)	-
PCL	-	52.69 (61.50)	-	35.80 (-68.104)
Ecoflex®	-	-	119.82 (0.54)	-
L,D-PLA:5CB	36.95 (0.29)	135.23 (5.15)	36.88 (0.25)	-
PCL:5CB	-	44.98 (63.21)	-	31.42 (-64.490)
Ecoflex® :5CB	-	-	105.38 (0.76)	-
L,D-PLA:SWCN	52.41 (0.38)	140.96 (12.12)	48.42 (0.34)	-
PCL:SWCN	-	53.51 (64.06)	-	45.47 (-63.175)
Ecoflex®:SWCN	-	-	126.14 (0.30)	-
L,D-PLA:5CB:SWCN	34.84 (0.28)	132.48 (10.95)	31.45(0.31)	-
PCL:5CB:SWCN	-	46.25 (62.06)	-	40.24 (-61.151)
Ecoflex®:5CB:SWCN	-	-	119.72 (0.24)	-

Temperatures in the DSC thermograms obtained during the second heating and cooling cycles at a heating/cooling
rate of 10 °C/min.
All investigated polymers and hybrid compositions give, under the second heating and cooling
cycles at 10 °C/min rate, various DSC profiles with melting/crystallization Tonset and glass transition
Tg temperatures more or less visible. These findings clearly indicate their semi-crystalline nature.
The glass transition temperature Tg of the investigated polymers was found for L,D-PLA during

Materials 2020, 13, 2480
7 of 20
heating and cooling and for Ecoflex® only during cooling; (see Table 1 and Figure 1 and Figure S1). It is
obvious that they depend on the structure of the polymers. First, wee noticed that: Ecoflex;® showed
signific antly higher Tg, consistent with thf ir more rigid chains. The addition of 5CB slightly detreased
the Tg of L,D-PLA and Ecoflex®. Tire opposite behavior was found for compositions of polymer:SWCN:
The addition of SWCN increased the Tg value for L,D-PLA and Ecoflex® i Quite different behavior,
depending on the polymer used, was found for the ternary compositions. in the case of L,D-PLA,
the addition of 0CB:SWCN decreased the value of Tg compared to the pure polymer and binary
compositions. Peculiar behavior wasnbserved for Ecoflex® :5CB:SWCN compositions when considering
the value of Tg. In this case, the value of T. Uor ternary composition was almost identical as that for fhe
pure polymer. In our opinion, this bohavior can be explaingd by the tact fhgt 5CB probably modified
the morpholopy oi the polymer (to make if moee homogeneous with a special track for SWCN) and
probably simplified the transfer of electrons in Ecoflex® due to the presence of SWCN.
Figure 1. Differential scanning calorimetry (DSC) curves with glass transition (Tg) registered during
heating (a) and cooling (b) for the created hybrid layers and pure L,D-poly(lactic acid).
All optical textures were registered at room temperature under a polarizing microscope with
crossed polarizers as well as without an analyzer (with one polarizer). The microphotographs taken
for the pure polymers and created hybrid layers are presented in Figure 2 and Figures S2 and S3 in
the Supplementary Materials. As one can see, the pure L,D-PLA layer is dark, while the admixtures
changed them signiffcantly (Figure 2). The admixture o f 5CB makes the texture celored, while after the
addition of SWCN, it becomes brighter. "Ternary hybrid layers were brighter and more coloeed when
comp ared with the layer of puro L,D-P LA.

Materials 2020,13,2480
8 of 20
Figure 2. Optical textures of pure; L,D-PLA and its hybrid layers registered -with crossed polarizers and
without an analyzer.
In the case of PCL, the addition of 5CB only makes the texture darker, as compared to tire
pure PCL layer, but the SWCN adminture completely changed the textures (Figure S2). A similar
influence of the admixtures was observed for the layers based on Ecoflex® (Figure S3). There was
no significant differences betwern the layers of neat Eroflex® and with the addition of 5CB, while
the SWCN admixture made; it significantly different. Summarizing the textute observations by POht,
the admixture of SWCN ha d a dominant imp, act on the morphology of the created hybrid layers of all
ob the studied polymers.
Moreover, simple optical microscope imaging was also done for all of the prepared samples (see
Figure S4). The most homogenous structure was observed for L,D-PLA (Figure S4A). "The presence ot
5CB in the proportion 1:10 to the polymer did not significantly change the registered images (Figure
S4D). The struchure of the film containtng O.Oi wgw of SWCN revealed a uniforts dispersion of smoll
nanotube domains within the pblymer matrix (Figure S4G). Art the amount of the SWCN increased,
the fiim bechme less transparent to iransmitted light, and the zone dominated by carbrn nanoparticles
increased (Figure S4J). Films made of pure PCL demonstsated a grain-like structure (Figure S4B),

Materials 2020,13,2480
9 of 20
which in the presence of 5CB was characterized by more dispersed and smaller domains (Figure S4E).
On the other hand, the addition of SWCN to PCL resulted in a heterogeneous texture with visible
zones of agglornerated nanotubes (Figure S4H,K). The optical micrographs for samples based on pure
Ecoflex® showed a homogenous structure (Figure S4C), while the addition of any additive caused
a large dispersion of blade spots (Figure S4F,I), which in the case of carbon nanotubes tend to form
agglomerates (Figure S4I).
The influence of the SWCN and/or 5CB on the surface topography of the biodegradable polymers
was additionally investigated by the AFM method (Figure 3). The morphplogy of the; pure L,D-PLA
surface was quite smooth and continuous with some irregular elevations up to 30 rum. PCL trep ted
regular mounds on .Ire surface, one next to the others. Ecoflex® has a tendency to create an oval
random cofl of a polymer chain. The addition of 5CB (10:1 w/w) changed the topography by making;
the structures bigger and higher, buC did not change the general character of the turface, while the
influence of SWCN was the most noticeable. In the case of PCL and Ecoflex®, both polymers covered
the crrbon nanotubes and the coating was latger for PCL than for Ecoflex®, which is clearly visible in
F°gure3. On tire other hand L,D-PLA chd not cover the r arbon nanotubes as effectively es PCL and
Ecoflex®, ond it is possible to notice single 1 gm length straight structures that came from the carbon
nanotubes. No significtnt changes between hybrid layers with gatbon nanotubes and with or without
5CB were observed for a°l three studiet1 polymers.
Figure 3. Atomic force microscopy (AFM) images of the pure studied polymers, binary, and ternary
hybrid layers.

Materials 2020,13,2480
10 of 20
The roughness parameters such as (Sa, Sq) for the investigated surfaces are presented in Table 2.
The presented parameters are defined in Equations (1) and (2):
where M and N are the total number of pixels in the analyzed scan; k and l are coordinates of a
given pixel; and z (xk, yi) is the height of the surface at a given coordinate. To determine the surface
parameters of the created layers, the most representative area of 20 pm X 20 pm, from each of the AFM
images presented in Figure 3, was selected for roughness analysis.
Table 2. The surface parameters of the polymers and hybrid compositions.
Surface Statistics :
Code	—
Sa (nm)	Sq	(nm)
L,D-PLA	1.27	2.12
PCL	31.26	43.78
Ecoflex®	12.74	17.28
L,D-PLA:5CB	0.80	1.44
PCL:5CB	84.20	109.40
Ecoflex®:5CB	25.13	35.59
L,D-PLA:SWCN	13.79	18.63
PCL:SWCN	56.38	75.13
Ecoflex®:SWCN	16.97	22.09
L,D-PLA:5CB:SWCN	21.56	28.18
PCL:5CB:SWCN	42.70	55.39
Ecoflex®:5CB:SWCN	11.29	14.91

* Values calculated for scanning field 20 pm X 20 pm (400 pm2 scan area).
The AFM study showed that all of the studied polymers exhibited various morphology depending
on the mixture composition. The mixture L,D-PLA with 5CB exhibited a root-mean-square (Sq)
roughness value of 1.44 nm, whereas the L,D-PLA:SWCN composition ca. 18.63 nm. The ternary
mixture based on L,D-PLA exhibited the highest value of Sq (28.18 nm) compared to the binary mixture
and pure L,D-PLA. The polymer L,D-PLA blended with 5CB contained less distinct features in the phase
separation morphology and exhibited a lower value of Sq compared to L,D-PLA, L,D-PLA:SWCN,
and L,D-PLA:5CB:SWCN. In the case of Ecoflex®, the following trend was found: 35.59 nm
(Ecoflex®:5CB) > 22.09 nm (Ecoflex®:SWCN) > 17.28 nm (Ecoflex®) > 14.91 nm (Ecoflex®:5CB:SWCN).
On the other hand, the mixture of PCL with additives showed a slightly different behavior (see Table 2),
which can probably be explained by the different miscibilities of all polymers with one or two additives.
In summary, the Sq parameter expresses the root mean square of deviations from the ideal plane,
so it can be assumed that for the created layers, the addition of 5CB does not change the surface
roughness (the order of magnitude Sq does not change, except PCL). In contrast, the addition of
SWCN caused an increase of Sq by one order of magnitude relative to the layer of pure polymer.
Therefore, nanotubes increased the surface roughness of composites, and their effect was similar in the
samples with and without the 5CB dopant.
## 3.2. UV-Vis Studies
The optical properties of polymers and hybrid compositions were investigated in chloroform
solution and in thin film by UV-Vis absorption spectroscopy. First, we investigated three biodegradable

Materials2020,13,2480
11 of20
polymers in chloroform by UV-Vis spectroscopy at various concentrations, monitoring the changes in
the n-n transitions. For L,D-PLA and PCL with concentrations of 500 mg/mL, the absorption curves
were; investigated for solutions diluted about 25-times, while for Ecoflex®, it was necessary to dilute
the solution 25,000 times. The UV-Vis absorption spectra of the polymers together with the calibration
curves are presented in Figure S5. Our study showed that with an increase in the concentration
of all investigated polymers, we did not observe changes in she maximum of the ebsorption band.
All investigated polymers exhibited one main absorption band tit about 230-240 tm. Moreover, for all
investigated polymers, the hyperchromic effect along with increasing eoncentration was observed.
The selected UV-Vis properties of the invnst igated polymers are jcresentod in Ttble S1.
In the next step* of our work, we investigated the UV-Vis properties of three biodegradable
polymers in thin film created by spin-coating anp drop-casting techniques. nn the spin-coating
Cechnique, we used 0.7 mL of polymer solution and created layers witn 650 rpm during 60 s. In the
drop-cast technique, we used 1 mL ot polymer solution. Photos of the created polymer layers are
presenied in Figure 4 and Figure S6.
Figure 4. Photos of the created polymer layers by the drop-casting method: polymers L,D-PLA (A),
PCL (B), Ecoflex® (A-C), polymers with 5CB in a ratio of 10:1 (w/w) (10-1-), pclymers with SWCN in a
ratio of 10:0.01 (w/w) (G-I), and polymers with SWCN in a ratio of 10:0.15 (w/w) (J,K).
The absorbance and transmittance of the thin created polymer layers are presented in Figure S7.
We did not observe big changes in the absorption band of the investigated polymers in the chloroform
solution and in thin films. As can be seen from the absorbance spectra for polymers, the absorption
bands lay below 300 nm, with the maxrna for L,D-PLA at 229 nm, PCL at 231? nm, and Ecoflee® at

Materials 2020,13,2480
12 of 20
266) nm, 284: nm, and 296 nm. Ecoflex® showed the highest absorbance out of all of the investigated
polymers. In the range from 350 nm to 1100 nm, L,D-PLA showed the highest transmittance equal to
90%, while the transmittance for PCL oscillated between 120-30% and for Ecoflex® between 20-60%,
increasing; its value to the highest wavelengths (see Figure S7).
To check the possibility o( using biodegradable polymees with SWCN and 5CB as transparent
and conductive anodes inorganic devices such as solar cells or light emitting diodes, in the next step,
we investigated the optical properties of the binary and tesoary mixlures in chloroform solution and as
a thin film. Photos of the prejsared binary and ternary eolutions are presented in lugure Se- UV-Vis
spectra of the binary and )ernary so(utions are presented in Figure 5 and Figure S9 together with the
calibration curves. As the weight ratio of 5CB and SWCN increased, no changes in the maximum oe thee
absorpsion bands of the investigated compositions were observed, only a hyperchromic effect existed.
Wavelength, nm
Wavelength, nm
(a)
#### (b)
Figure 5. UV-Vis absorption of tsrnary solutions based on Ecoflex® (al and L,D-PLA (b) where
A-E is Ecoflex:5CB:SWCN : (A) c (concentration) = 15.d mg/dm3 :c = 12.3 mg/dm3 :c = 8.7 mg/dm3; (B)
c = 30.3 mbdm3:c = 4.5 mg/dm3 :c = 17.3 mg/dm3 ; (C) c = 45.5 mg/dm3 :c = 6.21 mg/dm3 : c = 26.0 mg/dm3; (D)
c = 60 .6 mg/dm3:c = 9.1mg/dm3:c = 254.7 mg/dmx; (E) c = 175.8 mg/dm3:c = 11.3 mg/dm3:c = 43.3 mg/dm3.
(F-J) is L,D-PLA:5CB:SWCN: (IF) c = 21106.6 mg/dm3:c /= 2.3 mg/dm3 :c = 8.73 mg/dm3; (G)
c / 42112 m/dm/r 7= 4.6 id°/dm3:c = 17.1 mg/dm3 ; (H) r = 6319.8 mg/dmTc =/ 6.8 mg/dm3:c = 26.0 mg/dm3 ;
(I) c = 8426.4 mg/dm3:c = 9.1 mg/gmTc =/ 34:.7 mg/dm3; (J) c = 10533 mg/dm3 :c = 11.3mg/dm3:c = 43.3 mg/dm3.
For the ternary mixture (polymers and 5CB and SWCN), one isosbestic point was hound at
about 250 nm (Figure 6a and Figure S9), appearing as an effect of tha interactions between two or
theee compounds.
WEivdengfli, nm	Wavelenght, nm
#### (a) (b)
Figure 6. Absorption UV-Vis spectta of L,D-PLA and its compositions, 5CB ant;! SWCN in
chloroform with isosbestic points, where A—5CB; ((—SWCN; (2—L,D-PLA; D—L,D-dLA:5CB (900:1);
E—L,D-PLA;5CB (1)30:1:25.25) (a) pnd the transmittance of L,D-PLA and its compositions (b).

Materials 2020,13,2480
13 of 20
Ini the next step, the influence of 5CB and SWCN on the absorption properties of the polymer
layers was also determined by UV-Vis spectroscopy (Figure 6b). A general tendency was observed
regardless of the polymer used for layer composition. The addition of 5CB in an amount of 1:10 (w/a)
caused a bathochromic shift of both the absorbance and transmittance spectra by 70 nm, reaching
a wavelength value of 325) nm, which corsesponded to the rpectra of 5CB. in the case of L,D-PLA,
the presence of 5CB did not cause any additional charges rnthe spectral properties in the UV-Vis
range (Figure 6n). On the other hand, the addition of SWCN in the formed layer increased the baseline
in the absorbance; spectra and lowered tire transmtittance by 15%. Moreover, it corresponds well with
the amount of used SWCN, the higher the concentration, the greater the influence on the spectral
properties of the layer. The addition of SWCN to PCL slightly reduced the transmittance value by
about 5% at higher wavelength values. On the other hand, the absorption spectra only demonstrated
an inccement of fhe baseline with an increase in the portion of oWCN in the composition. In tire case of
Ecoflco®, the absorption spectra gave gn absorbance above 1 given the higher ihickness, which made it
difficult to analyze. Additionally, the transmittance was found bel ow 5%o for all compositi ons prepared
by ehe drop-c asting meehod.
Taking into consideration the transmittance of the created layers of the biodegradable polymers
with 5CB ann SWCN, we can nonclude that the 5CB admixture did ndt change the transmittsnce of the
investigated polymers, while the additidn of SWCN reduced the transmittance by approximately 15%>
fo5 L,D-PLA (see Figure 6b)r
Statistic Angle (Contact Measurement
Measurements of the static contact angle of the pelymer layer through o drop of water have shown
that all investigared polymers ore hydrophobic, wCh angle values ranging from H8° to 115)° (Table 0).
Thus, ehe application oh any aqueous solutions (e.g., PEDOT:PSS) will be problematic in terms of poor
interactions ond layer formation, as -will be shown below As can tie seen from Table3, the; presence of
5CB and SWCN in the fflm composition caused slight changes fn the contact angle value, however
maintainea the hydrophobic nature of the films (all tho values are above 100°).
Table 3. Results of the contact angle measurements for the polymer layers without and with additives.

Materials 2020,13,2480
14 of 20
Table 3. Cont.
In addition, for the Ecoflex® layers, with and without additives (5CB or SWCN), a rapid sorption
of deposited -water drop -was observed, as it is presented in Figure 7. A visible drop in the volume of
droplet -was observed for different time periods, starting from the moment the -water droplet came
into contact with the surface. The droplet spread completely over the film surface after five seconds
from deposition.

Materials 2020,13,2480
15 of 20
0.0 s	0.75	s	1.5	s	2.25 s	3.0	s	3.75	s	4.5	s	5.25	s
Figure 7. Selected images for the absorption process of water drop by? the Ecoflex® layer.
3.4. Infrared (IR) Thermography Study
The thermal behavior was studied for films composed of L,D-PLA, PCL and their mixtures with
5CB in ratio 10:1 w/w (polymer:5CB), and SWCN in ratios of 10:0.0x w/w or 10:0.5 w/w. The idea of this
study was to assess and select the film with the best (electrical properties, allowing its use as a flexible
electrode. It was not possible to deposit the poly(3,4-ethylenedioxythiophene):poly(styrenesulfonate)
(PEDOT:PSS) solution over our hybrid layers: in tire case of a water-based eolutlon, the hydrophobic
nature of the surface reduced the possiblo interaction causing pure or no surface ceverage, whereas the
use of the toluene-based solution caused the degradation of the composite layers structure (Figure 8).
(a)	(b)	(c)
Figure 8. Photo of L,D-PLA (a), PCL (b) and Ecoflcx® (c) with poly(3,4-
ethylenedioxythiophene):poly(styrenesulfonate) from water (left side) and toluene (right side).
Therefore, the general architecture of tested devices was a
PET/ITO/PEDOT:PSS/PTB7:PC70BM(1:1.5)/PFN/Ag/biodegradable polymer film, where L,D-PLA or
PCL as the cathode and encapsulated conductive materials were tested. Ecoflex® was not used in
this study given the unfavorable mechanical properties enabling handling while constructing the
device. In order to ensure the flexibility for all devices, commercial ITO-coated PET (poly(ethylene
terephthalate)) was used with a resistance a0-14 Q/square and transparency 70-72%. Resistivity of the
PEDOT:PSS was 500-5000 Q.cm.
The tests performed for layers based on L,D-PLA, PCL, L,D-PLA:5CB (10:1), and PCL:5CB (10:1)
behaved as electric insulators, as expected . The conductivity appeared when SWCN were present
in the polymer film sUructure. The lowest tested concentration iff carbon nanoUubes, 10:0.01 w/w for
polymer:SWCN, demonstrated a marginal current passage due to equipment limitations that were
unable to correctly assess its accuracy. The resistance for these fflms was above 100 MQ, hence no
change in the thermal images was noticed (see Figure 9 and Figure S10).
The increase in the SWCN amount from 0.01 to 0.5 significantly improved the conductivity only
in the case of L,D-PLA:SWCN (10:0.5), for which above 5 V, a current was measurable. Therefore, only
this composition was selected for thermal studies on a device with the architecture of a simple
solar cell presented in Figure 10, along with the results obtained for such a device. From the curve
current vs. potential, a significant difference in the observed current was noticed when compared to
the performance of L,D-PLA:SWCN (10:0.5) alone (see Figure 10a). The constant linear increase of
current upon increasing potential confirmed the conductive nature of the whole device, giving the
average resistance of 3030.7 Q. During whole experiment, the highest temperature reached was 53 °C
(Figure 10b).

Materials 2020,13, 2480
16 of 20
Figure 9). Thermal images for films conoposed of L,D-PLA, and PCI. with SWCN at the ratio 00:0.5 w/w
at 2.0 Va 6.0 V, and 10 .0 V.
(a)
# (b)
(c)
Figure 10. The architecture and photo of the created device and the summary of the thermal experiments for a
device composed of PET/lTO/PTB7:PCo0BM/PFN/Ag/L,D-PLA:SWCN (1.0:0.5) (red symbols): (a) corre)atioo
of the current versus applied potential (blue symbols for film LD-PLA :SWCN (10:0 .15)); (b) correlation of
temperature versus applied potential; (c) thermal images foo devices at 2,4, 6, S) and 1° V.

Materials 2020,13,2480
17 of 20
It should be stressed that in the IR thermography study, we did not use an external source of light.
We used an external source of the potential in order to induce thermal response due to current passage to
unveil the structural defects. The usage of an external light source could reduce the correct measurement.
##### 4. Summary and Conclusions
In this paper, we showed for the first time a comparative study of three different biodegradable
polymers (L,D-PLA, PCL, and Ecoflex®) in binary and ternary compositions with 5CB or/and SWCN.
We investigated the possibility of biodegradable polymer layers as electrodes (anodes and cathodes) in
polymer solar cells. For this purpose, we evaluated the conductivity of the hybrid layers consisting of a
biodegradable polymer with 5CB in a ratio of 10:1 and polymer:5CB:SWCN in a ratio of 10:1:0.01, and found
that both types of layers were transparent but not conductive. With an increase in the amount of SWCN to
5.in the composition, the conductivity of the layer only increased for L,D-PLA, losing transparency.
We also checked the usage of the investigated polymers as a biodegradable substrate instead of
PET with the conductive polymer PEDOT:PSS as the anode. Our study showed that all investigated
biodegradable polymers were hydrophobic, therefore it was not possible to form PEDOT:PSS layers
from toluene or the aqueous solution. Although Ecoflex® exhibited the best hydrophilic properties,
it showed the worst film-forming abilities among all of the investigated biodegradable polymers.
In summary, our study showed that of the three investigated biodegradable polymers, L,D-PLA
with the SWCN admixture exhibited the best electrical, optical, and thermal properties for use as part
of organic devices (e.g., solar cells, light emitting devices). However, technical modifications and
optimization of the layer preparation process are still required to obtain layers of L,D-PLA:SWCN
that are more homogeneous and without structural defects. New ideas for SWCN dispersion in a
polymer matrix are still needed, because the conductivity and mechanical properties of the hybrid
layer depend on it, and hence obtaining a biodegradable, conductive, and flexible polymer layer with
a low percolation threshold [16].
Finally, the following main conclusions can be formulated:
1. All investigated polymers and hybrid compositions exhibited a semi-crystalline nature with
   melting/crystallization and glass transition temperatures more or less visible. Addition of SWCN
   increased the Tg for L,D-PLA and Ecoflex®. In the case of L,D-PLA, the addition of both 5CB
   and SWCN decreased the Tg compared to the pure polymer and binary compositions. For the
   Ecoflex®:5CB:SWCN compositions, the Tg was almost identical as that for the pure polymer.
   The addition of 5CB to the polymer layer made it more homogeneous with a special track for
   SWCN and probably simplified the electron transfer in Ecoflex® due to the presence of SWCN.
2. Texture observations by POM showed that the admixture of SWCN had a dominant impact for
   morphology of the created hybrid layers of all studied polymers. On the other hand, no significant
   changes in the topography of hybrid layers with or without carbon nanotubes and 5CB were
   observed for all three polymers studied by the AFM method.
3. No changes in the maximum of absorption bands of the investigated compositions were observed,
   only the hyperchromic effect with the increase in 5CB and SWCN content.
4. The 5CB admixture did not change the transmittance of the investigated polymers while the
   addition of SWCN reduced it by approximately 15% in the case of L,D-PLA.
5. It turns out that all investigated polymers were hydrophobic and it was not possible to form
   PEDOT:PSS layers from toluene or an aqueous solution. Moreover, for the Ecoflex® layers, with
   and without additives, a rapid sorption of the deposited water drop was observed.
6. The resistance of the polymer:SWCN composition in a ratio of 10:0.01 w/w was above 100 MQ,
   hence no change in the thermal images was noticed. The increase in SWCN content from
   0.01 to 0.5 significantly improved the conductivity only in the case of the L,D-PLA:SWCN (10:0.5)
   composition, for which a current above 5 V was registered with a resistance of 3030.7 Q.

Materials 2020,13,2480
18 of 20
Supplementary Materials: The following are available online at http://www.mdpi.com/1996-1944/13/11/2480/s1,
Figure S1: DSC curves registered during heating and cooling rate of 10 °C/min for created hybrid layers and
pure polymers, Figure S2: Optical textures of pure PCL and its hybrid layers registered with crossed polarizes
and without analyser, Figure S3: Optical textures of pure Ecoflex® and its hybrid layers registered with crossed
polarizes and without analyser, Figure S4: Microscope images of layers with optical magnification of 18x:
polymers L,D-PLA, PCL, Ecoflex® (A, B, C), polymers with 5CB in a ratio of 10:1 (w/w) (D, E, F), polymers with
SWCN in a ratio of 10:0.01 (w/w) (G, H, I) and polymers with SWCN in a ratio of 10:0.5 (w/w) (J, K), Figure S5:
Concentration-dependent solution UV-Vis spectra of the polymers (a, c, e) together with calibration curves (b,
d, f)., Figure S6: Photos of polymer layers prepared by the spin-coating method, Figure S7: Absorbance and
transmittance of polymer layers of L,D-PLA (a), PCL (b), Ecoflex® (c) created by spin-coating, Figure S8: Photos
of polymers (A), polymer:5CB (B), polymer:SWCN (C, D) in chloroform solution, Figure S9: Binary and ternary
UV-Vis absorption solutions of polymer:5CB (a, b, c) and polymer:5CB:SWCN (d) compositions in chloroform
solution together with calibration curves (e-j). UV-Vis spectra of polymers, 5CB and SWCN in chloroform with
isosbestic points (k, l), Figure S10: Thermal images for films composed of on L,D-PLA, PCL, Ecoflex® (a) and
their selected mixtures with 5CB or SWCN (b), at 2.0 V, 6.0 V and 10.0V, Table S1: Selected UV-Vis properties of
polymers and binary and ternary compositions.
Author Contributions: Conceptualization, P.F. performed and analyzed DSC, POM and AFM experiments; K.A.B.
and B.J. performed the UV-Vis in thin film and contact angle experiments; K.A.B. and W.P. and B.J. performed and
analyzed the thermal imaging experiments; A.G. and R.P. performed and analyzed the UV-Vis in solution; M.M.
analyzed DSC and POM experiments, supervision, writing-Reviewing and editing; A.I. writing-original draft
preparation, supervision, writing-Reviewing and editing, conceptualization. All authors have read and agreed to
the published version of the manuscript.
Funding: The European Regional Development Fund in the framework of the Polish Innovation Economy
Operational Program contract no. POIG.02.01.00-12-023/08 (DSC 8000 Calorimeter). Financial support of Ministry
of Science and Higher Education (grant no. 2019-N17/MNS/000020) is acknowledged.
Conflicts of Interest: The authors declare no conflict of interest.
References
1. Li, R.; Wang, L.; Kong, D.; Yin, L. Recent progress on biodegradable materials and transient electronics.
   Bioact. Mater. 2018, 3, 322-333. [CrossRef] [PubMed]
2. Feig, V.R.; Tran, H.; Bao, Z. Biodegradable polymeric materials in degradable electronic devices. ACS Cent. Sci.
   2018, 4, 337-348. [CrossRef] [PubMed]
3. Chen, L.; Pang, X. The assembly of C60 in semicrystalline PLLA matrix. Nano-Micro Lett. 2012, 4, 30-33.
   [CrossRef]
4. Liang, B.; Zhang, Z.; Chen, W.; Lu, D.; Yang, L.; Yang, R.; Zhu, H.; Tang, Z.; Gui, X. Direct patterning of carbon
   nanotube via stamp contact printing process for stretchable and sensitive sensing devices. Nano-Micro Lett.
   2019,11,1-11. [CrossRef]
5. Slabov, V.; Kopyl, S.; dos Santos, M.P.S.; Kholkin, A.L. Natural and eco-friendly materials for triboelectric
   energy harvesting. Nano-Micro Lett. 2020,12, 42. [CrossRef]
6. Nagarajan, V.; Mohanty, A.K.; Misra, M. Perspective on polylactic acid (PLA) based sustainable materials for
   durable applications: Focus on toughness and heat resistance. ACS Sustain. Chem. Eng. 2016, 4, 2899-2916.
   [CrossRef]
7. Mallegni, N.; Phuong, T.V.; Coltelli, M.B.; Cinelli, P.; Lazzeri, A. Poly(lactic acid) (PLA) based tear resistant
   and biodegradable flexible films by blown film extrusion. Materials 2018,11,148. [CrossRef]
8. Zeng, J.B.; Li, K.A.; Du, A.K. Compatibilization strategies in poly(lactic acid)-based blends. RSC Adv. 2015, 5,
   32546-32565. [CrossRef]
9. Chee, W.K.; Lim, H.N.; Zainal, Z.; Huang, N.M.; Harrison, I.; Andou, Y. Flexible graphene-based
   supercapacitors: A review. J. Phys. Chem. C 2016,120, 4153-4172. [CrossRef]
10. Amjadi, M.; Yoon, Y.J.; Park, I. Ultra-stretchable and skin-mountable strain sensors using carbon
    nanotubes-Ecoflex nanocomposites. Nanotechnology 2015,26, 375501. [CrossRef]
11. Lee, J.W.; Xu, R.; Lee, S.; Jang, K.I.; Yang, Y.; Banks, A.; Yu, K.J.; Kim, J.; Xu, S.; Ma, S.; et al. Soft, thin
    skin-mounted power management systems and their use in wireless thermography. Proc. Natl. Acad.
    Sci. USA 2016,113, 6131-6136. [CrossRef] [PubMed]

Materials 2020,13,2480
19 of 20
1. Bogdanowicz, K.A.; Iwan, A.; Caballero-Briones, F.; Barceinas-Sanchez, J.; Przybył, W.; Januszko, A.;
   Miranda, J.B.; Espinosa-Ramirez, A.; Guerrero-Contreras, J. Optical and electrical properties of graphene
   oxide and reduced graphene oxide films deposited onto glass and Ecoflex® substrates towards organic solar
   cells. Adv. Mater. Lett. 2018, 9, 58-65. [CrossRef]
2. Tsuji, H. Polylactides. In Biopolymers, Polyesters III—Application and Commercial Product; Doi, Y., Steinbuchel, A.,
   Eds.; Wiley-Blackwell: New Jersey, NJ, USA, 2002; Volume 4, pp. 1-398.
3. Fryń, P.; Bogdanowicz, K.A.; Górska, N.; Rysz, J.; Krysiak, P.; Marzec, M.; Marzec, M.; Iwan, A.; Januszko, A.
   Hybrid materials based on L,D-poly(lactic acid) and single-walled carbon nanotubes as flexible substrate for
   organic devices. Polymers 2018,10,1271. [CrossRef]
4. Fryn, P.; Bogdanowicz, K.A.; Krysiak, P.; Marzec, M.; Iwan, A.; Januszko, A. Dielectric thermal and mechanical
   properties of L,D-poly(lactic acid) modified by 4'-pentyl-4 biphenylcarbonitrile and singlewalled carbon
   nanotube. Polymers 2019,11,1867. [CrossRef]
5. Ma, P.; Lv, P.; Xu, P.; Du, M.; Zhu, H.; Dong, W.; Chen, M. Design of bio-based conductive and fast
   crystallizing nanocomposites with controllable distribution of multiwalled carbon nanotubes via interfacial
   stereocomplexation. Chem. Eng. J. 2018, 336, 223-232. [CrossRef]
6. Shi, S.; Chen, Y.; Jing, J.; Yang, L. Preparation and 3D-prmtmg of highly conductive polylactic acid/carbon
   nanotube nanocomposites: Via local enrichment strategy. RSC Adv. 2019, 9, 29980-29986. [CrossRef]
7. Zare, Y.; Rhee, K.Y. Following the morphological and thermal properties of PLA/PEO blends containing
   carbon nanotubes (CNTs) during hydrolytic degradation. Compos. Part B Eng. 2019,175,107132. [CrossRef]
8. Liu, Y.; Zhang, W.; Zhang, F.; Leng, J.; Pei, S.; Wang, L.; Jia, X.; Cotton, C.; Sun, B.; Chou, T.W.
   Microstructural design for enhanced shape memory behavior of 4D printed composites based on carbon
   nanotube/polylactic acid filament. Compos. Sci. Technol. 2019,181,107692. [CrossRef]
9. Zhou, Y.; Lei, L.; Yang, B.; Li, J.; Ren, J. Preparation and characterization of polylactic acid (PLA) carbon
   nanotube nanocomposites. Polym. Test. 2018, 68, 34-38. [CrossRef]
10. Yang, L.; Li, S.; Zhou, X.; Liu, J.; Li, Y.; Yang, M.; Yuan, Q.; Zhang, W. Effects of carbon nanotube on the
    thermal, mechanical, and electrical properties of PLA/CNT printed parts in the FDM process. Synth. Met.
    2019, 253,122-130. [CrossRef]
11. Liu, S.; Wu, G.; Chen, X.; Zhang, X.; Yu, J.; Liu, M.; Zhang, Y.; Wang, P. Degradation behavior in vitro of
    carbon nanotubes (CNTs)/poly(lactic acid) (PLA) composite suture. Polymers 2019,11,1015. [CrossRef]
12. Li, M.Q.; Wu, J.M.; Song, F.; Li, D.D.; Wang, X.L.; Chen, L.; Wang, Y.Z. Flexible and electro-induced shape
    memory poly(Lactic Acid)-based material constructed by inserting a main-chain liquid crystalline and
    selective localization of carbon nanotubes. Compos. Sci. Technol. 2019,173,1-6. [CrossRef]
13. Babu, S.S.; Kalarikkal, N.; Thomas, S.; Radhakrishnan, E.K. Enhanced antimicrobial performance of
    cloisite 30B/poly (e-caprolactone) over cloisite 30B/poly (L-lactic acid) as evidenced by structural features.
    Appl. Clay Sci. 2018,153,198-204. [CrossRef]
14. Urquijo, J.; Dagreou, S.; Guerrica-Echevarrfa, G.; Eguiazabal, J.I. Morphology and properties of electrically
    and rheologically percolated PLA/PCL/CNT nanocomposites. J. Appl. Polym. Sci. 2017,134,1-10. [CrossRef]
15. Gopinathan, J.; Pillai, M.M.; Elakkiya, V.; Selvakumar, R.; Bhattacharyya, A. Carbon nanofillers incorporated
    electrically conducting poly e-caprolactone nanocomposite films and their biocompatibility studies using
    MG-63 cell line. Polym. Bull. 2016, 73,1037-1053. [CrossRef]
16. Babu, S.S.; Mathew, S.; Kalarikkal, N.; Thomas, S.; Radhakrishnan, E.K. Antimicrobial, antibiofilm,
    and microbial barrier properties of poly (e-caprolactone)/cloisite 30B thin films. 3 Biotech. 2016, 6, 249.
    [CrossRef]
17. Deliormanli, A.M.; Atmaca, H. Prechondrogenic ATDC5 cell response to graphene/multi-walled carbon
    nanotube-containing porous polycaprolactone biocomposite scaffolds. Int. J. Polym. Mater. Polym. Biomater.
    2019, 68,1154-1166. [CrossRef]
18. Gopinathan, J.; Pillai, M.M.; Sahanand, K.S.; Rai, B.K.D.; Selvakumar, R.; Bhattacharyya, A. Synergistic effect
    of electrical conductivity and biomolecules on human meniscal cell attachment, growth, and proliferation in
    poly-e-caprolactone nanocomposite scaffolds. Biomed. Mater. 2017,12,65001. [CrossRef]
19. Fortunati, E.; D'Angelo, F.; Martino, S.; Orlacchio, A.; Kenny, J.M.; Armentano, I. Carbon nanotubes and
    silver nanoparticles for multifunctional conductive biopolymer composites. Carbon 2011, 49, 2370-2379.
    [CrossRef]

Materials 2020,13, 2480
20 of 20
1. Dottori, M.; Armentano, I.; Fortunati, E.; Kenny, J.M. Production and properties of solvent-cast
   poly(e-caprolactone) composites with carbon nanostructures. J. Appl. Polym. Sci. 2011, 119, 3544-3552.
   [CrossRef]
2. Hu, L.; Hecht, D.S.; Gruner, G. Carbon nanotube thin films: Fabrication, properties, and applications.
   Chem. Rev. 2010,110,5790-5844. [CrossRef] [PubMed]
3. Zhu, H.; Wei, J.; Wang, K.; Wu, D. Applications of carbon materials in photovoltaic solar cells. Sol. Energy
   Mater. Sol. Cells 2009, 93,1461-1470. [CrossRef]
4. Jariwala, D.; Sangwan, V.K.; Lauhon, L.J.; Marks, T.J.; Hersam, M.C. Carbon nanomaterials for electronics,
   optoelectronics, photovoltaics, and sensing. Chem. Soc. Rev. 2013, 42, 2824-2860. [CrossRef] [PubMed]
5. Po, R.; Carbonera, C.; Bernardi, A.; Tinti, F.; Camaioni, N. Polymer- and carbon-based electrodes for polymer
   solar cells: Toward low-cost, continuous fabrication over large area. Sol. Energy Mater. Sol. Cells. 2012,100,
   97-114. [CrossRef]
6. Wu, Z.; Chen, Z.; Du, X.; Logan, J.M.; Sippel, J.; Nikolou, M.; Kamaras, K.; Reynolds, J.R.; Tanner, D.B.;
   Hebard, A.F.; et al. Transparent, conductive carbon nanotube films. Science 2004, 305,1273-1276. [CrossRef]
7. Cai, W.; Gong, X.; Cao, Y. Polymer solar cells: Recent development and possible routes for improvement in
   the performance. Sol. Energy Mater. Sol. Cells 2010, 94,114-127. [CrossRef]
8. Jewłoszewicz, B.; Bogdanowicz, K.; Przybył, W.; Iwan, A.; Plebankiewicz, I. PEDOT:PSS in Water and Toluene
   for Organic Devices—Technical Approach. Polymers 2020,12, 565. [CrossRef]
© 2020 by the authors. Licensee MDPI, Basel, Switzerland. This article is an open access
article distributed under the terms and conditions of the Creative Commons Attribution
(CC BY) license (http://creativecommons.org/licenses/by/4.0/).