Phase Polymorphism of [Mn(DMSO)6](ClO4)2 Studied by Differential Scanning Calorimetry
Anna Migdał-Mikuli and Elz˙bieta Szostak
Department of Chemical Physics, Faculty of Chemistry, Jagiellonian University, ulica Ingardena 3, 30-060 Krako´w, Poland
Reprint requests to Dr. hab. A. M.-M.; Fax: +48-12-634-0515; E-mail: migdalmi@chemia.uj.edu.pl
Z. Naturforsch. 60a, 289 – 295 (2005); received January 13, 2005

Six solid phases of [Mn(DMSO)6](ClO4)2 have been detected by differential scanning calorimetry. The phase transitions were found between the following solid phases: stable KIc stable KIb at TC5 = 225 K, metastable KIII metastable KII at TC4 = 322 K, stable KIb stable KIa at TC3 = 365 K, metastable KII overcooled K0 at TC2 = 376 K and stable KIa stable K0 at TC1 = 379 K. The title compound melts at Tm = 488 K.
↔	→
↔	→
↔
Key words: Hexadimethylsulphoxidemanganese(II) Chlorate(VII); Phase Transitions; Melting Point; DSC.

## Introduction
Hexadimethylsulphoxidemanganese(II)	chlorate
(VII) (called HMnC) consists of two ions: [Mn- ((CH3)2SO)6]2+ and ClO4−. The cation is a slightly deformed octahedron, where the manganese atom is surrounded by six oxygen atoms coming from the dimethylsulphoxide (DMSO) ligands. The DMSO ligands are built like C2v pyramids. So far the crys- tal structure of HMnC is unknown. However, the analogous compound [Cd(DMSO)6](ClO4)2 crystal- lizes in the rhombic system (space group: No 43; Fdd2; C19 [1]). We have recently investigated the polymorphism of [Cd(DMSO)6](ClO4)2 (HCdC) and [Co(DMSO)6](ClO4)2 (HCoC) by differential scanning calorimetry (DSC) [2, 3], and found that both substances have five solid phases. Three of them are stable and two are metastable phases. The high temperature phases of these compounds can be easily overcooled. The purpose of the present work was to carefully examine the polymorphism of HMnC in the temperature range of 173 – 530 K using DSC. Additionally, we compared the obtained results with those obtained earlier for HCdC [2] and HCoC [3].
2v
## Experimental
  1. Sample Preparation
A few grams of [Mn(H2O)6](ClO4)2 were dissolved while being slowly heated up in DMSO of high chem- ical purity, which was previously additionally purified
by vacuum distillation at low pressure and next was dehydrated by shaking with anhydrous CaH 2, accord- ing to requirements presented in [4]. This solution was then chilled and the precipitated crystals of HMnC were filtered and washed with acetone. They were then dried in a desiccator over phosphorous pentaoxide for a few hours. After desiccation, they were put in a sealed vessel and stored in a desiccator with barium oxide as a desiccant.
To check the chemical composition of the synthe- sised HMnC, the percentage content of manganese ions was checked using a complexometric method, with a solution of the sodium salt of ethylenedi- aminetetraacetic acid (EDTA) as a titrant. The theo- retical content of manganese equalled 7.60%, and its content found by the titration analysis amounted to
7.51 0.18%. The content of carbon and hydrogen in the DMSO ligand was determined using elemen- tary analysis on an EURO EA 3000 apparatus. For carbon atoms, the difference between the theoretical value (19.95%) and the test value (19.31 0.01%) did not exceed 0.1%. For hydrogen atoms, the theoretical value was 5.02% and the test value was 5.16 0.01%. Therefore, the elementary analysis of the title com- pound confirmed the presence of the stoichiometric number of six DMSO molecules in the complex cation.
±
±
±

  1. Sample Identification and Characteristics
In order to further identify the title compound, its infrared absorption spectra (FT-FIR and FT-MIR) and

0932–0784 / 05 / 0400–0289 $ 06.00 Oc 2005 Verlag der Zeitschrift fu¨r Naturforschung, Tu¨bingen · http://znaturforsch.com

Fig. 1. Comparison of the infrared (FT-FIR and FT-MIR) and Raman (FT-RS) spectra of [Mn(DMSO)6](ClO4)2.

its Raman spectrum (FT-RS) were recorded at am- bient temperature. The FT-FIR and FT-MIR spectra were obtained using Digilab FTS-14 and EQUINOX- 55 Bruker Fourier transform infrared spectrometers, respectively, with a resolution of 2 cm−1. For pow- der samples, suspended in apiezon grease, the FT-FIR spectrum was recorded using polyethylene and sili- con windows. The FT-MIR spectrum was recorded for a sample suspended in Nujol between the KBr pellets. The FT-RS spectrum was recorded using a Bio-Rad spectrometer with a YAG neodymium laser ( = 1064 nm) at 10 – 4000 cm −1 at a resolution of 4 cm−1. Figure 1 presents a comparison of the infrared and Raman spectra of HMnC. Table 1 contains a list of the obtained and literature data [2 – 8] of band fre- quencies and their assignments. The recorded spec- tra additionally identify the investigated compound as [Mn(DMSO)6](ClO4)2.
Thermal analysis of the examined compound was made in order to enable further verification of its com-
Table 1. The list of band positions of the Raman (FT- RS) and infrared spectra (FT-FIR and FT-MIR) of solid [Mn(DMSO)6](ClO4)2 and liquid DMSO at room temper- ature (vw, very weak; w, weak; sh, shoulder; m, medium; st, strong; vst, very strong; br, broad).

Frequencies in cm−1 [Mn(DMSO)6](ClO4)2	DMSO
RS	IR	RS	IR	Assignments
this work this work	this work	[4, 5] in KBr a in Apiezon
pellet	b in Nujol

68 wa	L (lattice)
77 wa	L (lattice)
116 m	103 sha	L (lattice)
134 wa	L (lattice)
168 ma	d(MnO)
197 vw	216 sta	d(MnO)
314 m	316 ma	313 m 313 w as(CSC)
343 m	344 sta	338 m 338 m as(CSO)
388 m 381 m s(CSO)
403 w	s(CdO)
419 m	418 ma,b	as(MnO) 459 m	d(OClO) E
625 m 628 m 624 mb	d(OClO) F2
662 vwb	612 sh s(CS)
679 vst 678 w 677 wb	663 vst 663 m s(CS)
714 st 714 m 717 mb	700 m 700 st as(CS)
910 w 904 w	900 vw 900 w (CH3)
934 vst 941 sh	s(ClO) A1
941 stb	925 vw 931 m (CH3)
962 w 955 st 952 stb	954 w 955 st (CH3)
1006 w	995 stb	(CH3)
1028 m 1011 vst 1012 stb	s(SO)
1042 m	1039 shb 1050 m 1050 vst s(SO)
1096 m 1100 sh 1098 vstb	d(ClO) F2
1123 st	1126 vstb	d(ClO) F2
1297 vw 1299 shb	1303 m s(HCH)
1318 m	1319 mb	1313 w	s(HCH)
1384 vw 1377 mb	as(HCH)
1422 st 1416 m 1414 shb	1404 st as(HCH)
1437 m	1456 vstb	1425 m 1440 st as(HCH)
2816 sh	2857 vstb 2885 br 2825 br s(CH)
2867 sh	2870 shb	s(CH)
2922 vst 2917 m 2922 vstb 2913 vst 2910 st s(CH)
2958 vstb	as(CH)
2995 sh	2999 m 2999 st as(CH)
3009 st 3000 m 3008 mb	as(CH)

position. The thermogravimetric (TG) measurements and simultaneous differential thermal analysis (DTA) were performed using a Mettler Toledo TGA/SDTA 851e apparatus. A sample weighing 10.9628 mg was placed in a 150 l Pt/Rh crucible. The TG measure- ments were made in a flow of argon (80 ml/min) from 303 K up to 393 K at a constant heating rate of 2 K min−1. The simultaneous evolved gas analysis (SEGA), with an on-line quadrupole mass spectrome- ter (QMS) using a Balzer GSD 300T apparatus, was
Table 2. Thermodynamics parameters of the detected phase transitions (on heating).
[Mn(DMSO)6](ClO4)2
Tc	H	S
K	kJ mol−1	J mol−1 K−1

Tm	487.65 ± 3.00	37.83 ± 1.30	184.48 ± 2.90
TC1	378.66 ± 1,10	3.43 ± 0.40	9.07 ± 1.06
TC2	375.66 ± 2.25	4.44 ± 0.45	11.83 ± 1.21
TC3	364.66 ± 3.00	27.11 ± 1.24	74.33 ± 2.86
TC4	321.56 ± 2.53	16.60 ± 0.62	51.63 ± 1.82
TC5	225.40 ± 0.09	0.88 ± 0.11	1.99 ± 0.25

(QMS) and chemical analysis have jointly certified the purity and proper composition of the examined com- pound. However, it should be stressed that the inves- tigated compound is not very stable and starts losing (CH3)2SO molecules, already at room temperature, of course when it is not hermetically confined.

Fig. 2. TG, DTG, QMS and SDTA curves for HMnC at 303 – 393 K. (a, signal of m/e = 18; b, m/e = 17; c, m/e = 16; d, m/e = 48; e, m/e = 14; f, m/e = 44; g, m/e = 13; h, m/e = 15;
i, m/e = 32; j, m/e = 64).
also registered. The temperature was measured by a Pt-Pt/Rh thermocouple with an accuracy of 0.5 K. Figure 2 presents a comparison of the TG, DTG, QMS and SDTA curves for HMnC within the temperature range of 300 – 380 K. For reasons of graphic clarity, only the masses of m/e = 13, 14, 15, 16, 17, 18, 32,
±
44, 48 and 64 – representing the fragments: CH, CH 2, CH3, CH4 or O, OH, H2O, S or O2, CO2, SO and
SO2 [of (CH3)2SO fragmentation] are shown. It can be seen from TG and DTG curves that during heating from RT up to 393 K the sample does not lose more than ca. 2% of its initial mass. This means that the ti- tle compound practically does not change its chemi- cal composition in temperature range covering the de- tected phase transitions, even when the sample is not hermetically confined. Moreover, the absence of peaks both on QMS and on DTA curves, additionally con- firms that the statement presented above is true.
To sum up, the FT-RS, FT-FIR and FT-MIR spectra, the thermal analysis (TG, DTA), mass spectroscopy
  1. Heat Flow Measurements
The DSC measurements of HMnC were made using two types of DSC apparatus: the first one was a Perkin- Elmer DSC-7 apparatus used in the temperature range of 173 – 520 K for samples hermetically confined in 30 l aluminium containers. The weight of that sam- ple was 10.90 mg (sample a). Details of the DSC ex- periment are the same as described in [9]. The second one was a Perkin-Elmer PYRIS 1 DSC apparatus on which three samples were investigated in the temper- ature range of 173 – 400 K. The weight of these sam- ples was respectively: 16.16 mg (sample b), 6.32 mg (sample c) and 12.46 mg (sample d). The experimental details were the same as published in [10].

## Results and Discussion
The temperature dependencies of the difference in thermal power supplied to the two calorimeters (the so-called thermal stream or heat flow), named DSC curves, were obtained for each of four HMnC samples at different scanning rates and at different initial and final sample heating and cooling conditions. Masses of the samples were chosen as to determine whether the observed phase transition depended on the sample weight, or not. We did not notice significant differences between the results for the samples a, b, c and d. All thermodynamic parameters of the phase transitions are put together in Table 2. The results of all DSC mea- surements are schematically presented altogether as a temperature dependence of the free enthalpy G (Gibbs free energy) and shown in Figure 3.
Fig. 3. Scheme of the temperature dependence of the free enthalpy G of HMnC.

Fig. 4. DSC curves obtained during heating (curve No 1) and during cooling in the temperature range of 173 – 298 K (curve No 2) of HMnC with a scanning rate of 30 K/min.

All investigated samples, not yet subjected to any “thermal history”, so-called “virgins”, are in a crys- talline phase described as a KIb phase. The measure- ments on sample a were started by cooling the sample from room temperature (RT) to 173 K, holding it at this temperature for l min, then heating it up to 393 K and then cooling it again down to 173 K. The DSC curves obtained on first cooling (curve No 1) and subsequent heating (curve No 2) of sample a, with a scanning rate of 30 K/min, are shown in Figure 4. As can be seen in Fig. 4, during cooling and heating the sample a, dis- plays at ca. 225 K on both DSC curves a small exother- mic and endothermic anomaly, respectively, which is connected with the reversible solid phase transition: the KIb phase ↔ the KIc phase (compare with dia-

Fig. 5. DSC curves registered during heating from 293 to 393 K (curve No 3) and during cooling at 293 – 393 K (curve No 4) of HMnC with a scanning rate of 20 K/min.

gram in Fig. 3). This anomaly was recorded also for the “virgin” samples b and c, which were cooled down to 153 K and then heated up to 393 K. For sample d the anomaly was not recorded, probably because of the low value of the sample weight and too high value of the scanning rate (40 K/min). This transition tempera- ture was marked as TC5 = 225 K.
While heating sample b from 273 K till 393 K, be- ing initially in the KIb phase, it undergoes the phase transition at TC3 = 365 K into the KIa phase, which goes next at TC1 = 379 K into the K0 phase (compare with Fig. 3). Due to this transition, distinct anomalies on the DSC curves were recorded for all four samples a, b, c and d. For example, Fig. 5 shows these anoma- lies recorded at TC3 = 365 K and at TC1 = 379 K for sample b with a heating rate of 20 K/min (curve No 3). While cooling sample b in the K0 phase from 393 K till 273 K, a slight overcooling was observed. The over- cooled K0 phase undergoes the metastable phase at TC2 = 376 K, described as the KII phase. Being further cooled down, the KII phase goes next at TC4 = 322 K into the KIII phase (compare with Fig. 3). The phase transitions at TC2 and at TC4 were recorded on the DSC curves as anomalies connected with exothermic pro- cesses for all four samples a, b, c and d. For exam- ple, these two anomalies were showed for sample b in Fig. 5 (curve No 4).
The phase transitions from the overcooled K0 phase to the KII phase (at TC2) and from the KII phase to the KIII phase (at TC4) are reversible. This is clearly vis- ible in Fig. 6, showing for example DSC curves that

Fig. 6. DSC curves registered during heating from 293 to 393 K (curve No 5) and during cooling at 393 – 293 K (curve No 6) of HMnC with a scanning rate of 10 K/min.

Fig. 7. Comparison of the DSC curves registered during heat- ing from 298 to 393 K with a scanning rate of 30 K/min (curve No 7) and 40 K/min (curve No 8) in two different sets of measurement conditions.
were recorded during heating (curve No 5) and cool- ing (curve No 6) sample a in the temperature range of 293 – 393 K with a rate of 10 K/min. Both during heat- ing and cooling, two distinct anomalies on the DSC curves occured that were due to both detected phase transitions: the overcooled K0 phase KII phase and the KII phase KIII phase.
↔
↔
In order to better clarify the metastable character of phases KII and KIII, in Fig. 7 we have compared the DSC curves registered at two different initial condi- tions of the measurements. On the DSC curve No 7 we can see one major anomaly at TC4, connected with the transition from metastable phase KIII to metastable phase KII, and a doublet anomaly at TC3, connected
Fig. 8. Comparison of the DSC curves registered during heat- ing from 370 to 393 K with a scanning rate of 40 K/min at two different conditions of measurements.
with the phase transition stable phase KIb stable phase KIa and a single anomaly at TC2, connected with the phase transition metastable phase KII stable phase K0. On the DSC curve No 8 we can see one slight anomaly at TC4, connected with the phase tran- sition metastable phase KIII metastable phase KII, one major anomaly at TC3, connected with the phase transition stable phase KIb stable phase KIa and a slight one at TC1, connected with the phase transi- tion stable phase KIa stable phase K0. Curve No 7 was obtained during heating the sample immediately after cooling it to 193 K, whereas curve No 8 was obtained during heating the sample and also cooling down to 193 K but only after holding it at this tem- perature for 5 min. Thus, in this second case, because of the slow spontaneous conversion of a large part of the metastable phase KIII, first probably into the stable phase KIc and next into the stable phase KIb, we can see on curve No 8 the small anomaly at TC4 and big one at TC3, connected with the KIII KII and KIb KIa phase transitions, respectively. On curve No 7 quite an opposite phenomenon has occurred; one can observe a major anomaly at TC4 and a slight one at TC3, because in this case only a small part of the metastable phase KIII had converted into the stable phases KIc and/or next KIb. Moreover, on curve No 7 one can see only the anomaly at TC2, and one does not see the anomaly at TC1, whereas on curve No 8 the situation is reversed. This has occurred due to the fact that in the second case the metastable phase KII was partially converted into the stable KIb phase and afterwards completely converted into the KIa phase.
→
→
↔
→
→
→	→
In spite of very small differences between the phase transition temperatures and also of enthalpy changes,

Fig. 9. DSC curve registered in the temperature range of 420 – 520 K during heating of HMnC with a scanning rate of 25 K/min.
the phase transitions undergoing at TC2 and at TC1 con- sist actually of two different phase transitions. Namely: Fig. 8 presents the comparison of the two curves ob- tained at heating same sample c with the same scanning rate of 40 K min−1 but after two different “thermal his- tories”. On curve No 9 we can see the anomaly at TC2 connected with the KII K0 phase transition, because the sample was earlier cooled fast (30 K min−1) to the phase KII. On curve No 10 we can see an anomaly
→
at TC1 connected with the KIa K0 phase transition, because the sample was cooled slowly (10 K min−1) exactly as in phase KIa.
→
Of course it is not possible to determine the nature of the observed phases only on the basis of DSC measure- ments. However, it was observed with a microscope that all the phases proceed in the solid state. Moreover, it was verified by X-ray powder diffraction measure- ments, which are now in elaboration in order to deter- mine the crystal structure of all discovered phases of the title compound [11].
Additionally, it was concluded from the enthalpy change S at the TC3 and TC4 phase transitions (see Table 2), that the phases KII and KIa are in high rota- tional disorder, so that they are called “orientationally dynamically disordered crystals” (ODIC). The phases KIc, KIb, and K0 are more or less the ordered ones (small S values connected with the KIc KIb and KIa K0 phase transitions, registered at TC5 and TC1, respectively). The KIII and KII phases form mutually an enantiotropic system but, in a relation to the KIa, KIb and KIc phases, they are metastable in the whole
→
→
temperature range, and thus they form a monotropic system.
When heated up above TC1 the sample melts at Tm = 488 K. A subsequent DSC curve, showing the anomaly resulting from the melting process, can be seen in Fig. 9 (curve No 11).

## Conclusions
The thermodynamic parameters for the following phase transitions of HMnC have been determined:
reversible phase transition: stable KIc	stable KIb at TC5 = 225 K;
•	↔
reversible phase transition: metastable KIII metastable KII at TC4 = 322 K;
•	↔
irreversible phase transition: stable KIb	stable KIa at TC3 = 365 K;
•	→
reversible phase transition: metastable KII overcooled K0 at TC2 = 376 K;
•	↔
irreversible phase transition: KIa	K0 at TC1 =
•	→
379 K;
melting of the crystals at Tm = 488 K.
•
It can be concluded from the enthalpy values of the transitions, that the phases KII and KIa are phases of high rotational disorder [“orientationally dynami- cally disordered crystals” (ODIC)]. Phases KIc, KIb, and K0 are more or less ordered. Contrary to HCdC and HCoC the enthalpy change connected with the melting of HMnC is evidently higher than their values for the order-disorder phase transitions at TC3 and TC4.

Acknowledgements
Our thanks are due to Prof. Dr. S. Wro´bel from the Faculty of Physics, Astronomy and Applied Com- puter Science of the Jagiellonian University for en- abling us to perform the DSC measurements on the PYRIS 1 apparatus, and to Dr. hab. E. Mikuli from the Faculty of Chemistry of the Jagiellonian University
for stimulating discussions. We are also grateful to J. S´ ciesin´ski, M. Sc. and Dr. hab. E. S´ ciesin´ska from the
H. Niewodniczan´ski Institute of the Nuclear Physics Polish Academy of Sciences in Krako´w for the FT- FIR spectrum, to Dr. A. Wesełucha-Birczyn´ska from the Regional Laboratory of Physicochemical Analysis and Structural Research in Krako´w for the FT-RS spec- trum and Dr. M. Molenda from the Faculty of Chem- istry of the Jagiellonian University for his help in the thermal analysis of the title compound.
T. U. Lubeznowa and I. Ponomariew, Kristallografia
34, 862 (1989).
1. A. Migdał-Mikuli, E. Mikuli, E. Szostak, and J. Ser- won´ska, Z. Naturforsch 58a, 341 (2003).
2. A. Migdał-Mikuli and E. Szostak, Thermochim. Acta
426, 191 (2005).
1. J. Selbin, W. E. Bull, and L. H. Holmes Jr., J. Inorg. Nucl. Chem. 16, 219 (1961).
2. F. A. Cotton, R. Francis, and W. D. Horrocks Jr., J. Phys. Chem. 64, 1534 (1960).
3. M. Sandstro¨m, I. Persson, and St. Ahrland, Acta Chem. Scand. A 32, 607 (1978).
4. J. E. Connet, J. A. Creighton, J. H. S. Green, and
W. Kynaston, Spectrochim. Acta 22, 1859 (1966).
1. Raman/IR Atlas. Verlag Chemie, Weinheim/Berg- straße, Germany 1974.
2. E. Mikuli, A. Migdał-Mikuli, and J. Mayer, J. Thermal Anal. 54, 93 (1998).
3. A. Migdał-Mikuli, E. Mikuli, S. Wro´bel, and Ł. Hetman´czyk, Z. Naturforsch. 54a, 590 (1999).
4. A. Migdał-Mikuli, E. Szostak, M. Buc´ko, and
E. Mikuli, J. Solid St. Chem., in press.