European Polymer Journal 155 (2021) 110577
Double-stranded surface-grafted polymer brushes with ladder-like architecture
Artur J. Wo´jcik a, Karol Wolski a, Szczepan Zapotoczny a, b,*
a Faculty of Chemistry, Jagiellonian University, Gronostajowa 2, Krako´w 30-387, Poland
b Academic Centre for Materials and Nanotechnology, AGH University of Science and Technology, al. A. Mickiewicza 30, Krak´ow 30-059, Poland
A R T I C L E I N F O
A B S T R A C T
Keywords:
Double-stranded polymers Polymer brushes
Ladder-like brushes
Surface-initiated polymerization Bifunctional monomers
This feature paper focuses on recently introduced double-stranded surface-grafted polymer brushes with ladder- like architecture, the method of their synthesis, self-templating surface-initiated polymerization (ST-SIP), as well as their unique properties. ST-SIP synthetic approach is based on a sequential polymerization of a bifunctional monomer leading to formation of multimonomer chains in the first step followed by a second polymerization producing ladder-like structures. This approach was developed primarily for conjugated polymer brushes, which synthesis using other methods is challenging. Such brushes enable anisotropic conductance at the nanometer scale that is highly demanded for e.g., photovoltaic and optoelectronic applications. ST-SIP was applied to form ladder-like brushes containing polyacetylene, polythiophene and polyethynylpyridine conjugated chains ar- ranged normally to the grafting surface and exhibiting high electrical conductance as measured using conductive atomic force microscopy. The conjugated chains were shown to exhibit long term stability that is one of the crucial benefit of this novel brush topology. The nanomechanical characterization revealed enhanced stiffness and high elasticity of the ladder-like structures compared to the parent single-stranded brushes. The double- stranded brush topology due to anisotropic conductance, unique nanomechanical properties and versatility of ST-SIP approach, have a high potential for fabrication of robust nanocoating for tailoring (bio)interafaces.
1. Introduction
systems [6], organic transistors [7], optoelectronic devices [8,9]. However, their final applicability depends on many factors like thermal and air stability, spatial arrangement and conformation of polymer chains, mobility of charge carriers and a mechanism of charge transport, as well as presence of functional groups enhancing their solubility [10,11]. The main problems in applications of the conjugated polymers are related to poor solubility of pristine, unfunctionalized conjugated chains and high influence of chain disorder on conductivity of bulk and thin film systems [3]. While most of the current applications encompass the conjugated polymers in bulk or thin layers, the ultimate devices, e.g., ordered heterojunction solar cells or single-molecule electronics, would require platforms of conductive molecular wires arranged normally to a surface [12]. Such platforms would be also ideal systems for investiga- tion of charge transport on the molecular scale to achieve a fundamental understanding of the process [11,13].
Very promising structures that may address the mentioned issues are surface-grafted conjugated polymer brushes. They may offer an intra- molecular transport of charge carriers, along the ordered chains, that is more efficient than the intermolecular one [14]. Furthermore, they
Conjugated polymers,
like polyaniline, polythiophene, poly-
acetylene, poly(3,4-ethylenedioxythiophene) and poly(p-phenylene vinylene), are organic macromolecules with a backbone composed of alternating single and double bonds. In their native form, they are typically semiconductors with the conductivity values reaching
10-10-10-5 S/cm, but after incorporation of appropriate doping agents
(dopants, e.g. iodine ions) in the system of delocalized л-electrons, they reach conductivities typical for metals (102–105 S/cm) [1,2]. It is worth mentioning, that their electrical properties may be tuned via redox re-
actions by means of chemical or electrochemical methods, doping/ dedoping processes [3].
Thanks to their flexibility, relatively low cost of fabrication, broad range of possible chemical structures and architectures, and unique conductive properties, there is an increasing interest in synthesis of conjugated polymers for numerous applications. Native conjugated polymers and hybrid systems have found applications in fabrication of bioelectronics [4], superhydrophobic biointerfaces [5], light-harvesting
* Corresponding author at: Faculty of Chemistry, Jagiellonian University, Gronostajowa 2, Krako´w 30-387, Poland.
E-mail address: zapotocz@chemia.uj.edu.pl (S. Zapotoczny).
https://doi.org/10.1016/j.eurpolymj.2021.110577
Received 11 April 2021; Received in revised form 31 May 2021; Accepted 8 June 2021
0014-3057/© 2021 The Authors. Published by Elsevier Ltd. This is an open access article under the CC BY license (http://creativecommons.org/licenses/by/4.0/).
Available online 11 June 2021
Contents lists available at ScienceDirect

European Polymer Journal
journal homepage: www.elsevier.com/locate/europolj

A.J. Wo´jcik et al.

enable covalent connection of the chains and surfaces enhancing their stability and interfacial conductance offering also a precise control over the macromolecular architecture [15,16]. However, due to in- compatibility of classical polycodensation methods, commonly applied for syntheses of conjugated polymers, obtaining conjugated polymer brushes using surface-initiated polymerizations has been challenging leading to formation of such brushes only for selected monomers [2,17–19].
Polymer topology that may address some of the above-mentioned limitations is a double-stranded architecture. Double-stranded poly- mers consist of macromolecules having an uninterrupted sequence of rings with adjacent rings having at least one atom (spiro polymer) or more atoms in common (ladder polymer) [20]. The chains forming the double-stranded topology may differ in conjugation leading, in extreme case, to fully conjugated ladder polymers [21]. Generally, the ladder polymeric systems have been known for several decades and recently developed due to increasing interest related to their unique optoelec- tronic properties [22,23]. They can be synthesized using two general strategies: direct ladder polymerization of cyclic monomers or zipping of linear polymers containing polymerizable side groups (multimonomer) that are both challenging and commonly lead to defected ladder struc- tures due to e.g. branching and crosslinking. The covalently locked coplanar conformation of a conjugated ladder-type backbone, in contrast to conventional non-ladder polymers with relatively high torsional freedom, allows for extensive intrachain delocalization of molecular orbitals and transport of (quasi)particles such as charges, excitons, polarons, and spins. The rigid coplanar conformation can also enhance interchain electronic coupling of conjugated ladder polymers due to the small reorganization energy of a rigid system upon electron transfer or photoexcitation. It is worth mentioning, that non only coplanar conformation, but also helical conformation of conjugated ladder polymers may be obtained.
However, complex synthetic routes and limited solubility of such
rigid, coplanar ladder systems are challenging and limit their charac- terization, processing, formation of organized thin films, impeding also their applicability. Fabrication of surface-grafted polymer brushes with ladder-like (not only well-defined ladder structures) architecture may help to omit some of those problems thanks to inherent properties of the chains densely grafted to a surface.
This mini-review features novel double-stranded surface-grafted polymer brushes with ladder-like architecture, self-templating poly- merization approaches leading to such structures, their unique proper- ties and potential applications. The presented synthetic strategy was originally introduced to obtain conjugated brushes but it is very versa- tile and may be further extended to formation of complex topologies at surfaces with various functionalities and applications ranging from biosensors, fabrication of bioactive surfaces to flexible photovoltaics. We describe briefly also classical polymer brushes, synthetic strategies leading to them, and discuss unconventional polymer brush topologies but the main focus is on the synthesis and properties of ladder-like polymer brushes, the topology which was introduced in 2012 [30].
Polymer brushes

  1. General description
A term “polymer brushes” [24,25] typically refers to an array of polymer chains tethered to a surface by one end only, and so densely that they tend to adopt a stretched conformation. If the chains are anchored not to a surface but another polymer chain, such systems are typically distinguished as “bottlebrushes” [26] or “molecular brushes” [27].
While recently introduced advanced topological structures like loop and cyclic polymer brushes [28,29], ladder-like brushes [30] may not fully comply with the “classical” definition they certainly exhibit poly- mer brush properties related to surface tethering of a macromolecule at
European Polymer Journal 155 (2021) 110577

a single anchoring point only and sufficient packing of those macro- molecules to ensure their extended conformations.
The first general theoretical description of the polymer brushes appeared in works of De Gennes [31] and Alexander [32] and referred to linear chains polymer brushes. Later, the theoretical description also used the self-consistent field method [33–35] and Monte Carlo simula- tions [26]. Only recently, due to increasing interests in more sophisti- cated brush topologies, they have been also explored theoretically showing more complex behavior compared to linear polymer brushes [36]. The modelling typically results in obtaining density profiles of given brushes at certain conditions. However, in the case of relatively high values of the grafting density (number of polymer chains per unit area, σ) and for low molecular weight macromolecules, the obtained fits may deviates from the experimental results due to limitations of the models (e.g. not taking into account strong intermolecular interactions). A structural definition of the polymer brush regime based on a quantitative analysis of parameters like the distances between anchoring points (d), height of the brushes (H), bulk density of the brush (ρ), and number average molecular weight of the surface-grafted chains (Mn), was presented in 2007 [24]. Briefly, if a reduced grafting density (Σ, see Eqs. (1) and (2)) reaches the values less than 1, a non-(weakly)
interaction regime (the mushroom conformation) is observed; if Σ ≈ 1 –
a crossover regime is reached, and if Σ reaches clearly more than 1 (≫1), a highly stretched regime (the brush conformation) is observed.
(1)

(2)
Σ = σπR
2
g
σ = (HρNA)/Mn or σ = 1/d2
where Rg – radius of gyration of a tethered chain, NA – the Avogadro’s number.
While the abovementioned relations describing the mushroom-brush transition were derived for flexible linear polymer chains, semi-flexible or rod-like tethered chains were found to require smaller grafting den- sities for the brush formation compared to flexible chains [37] and more complex polymer topologies still need detailed theoretical modelling.
2.2. Classical synthetic approaches for polymer brushes

Polymer brushes have been obtained so far on numerous substrates with various compositions and shapes including convex [38] and concave [39] structures. Typically metals and oxides like gold [40], iron oxides [41], titanium dioxide [42], indium tin oxide (ITO) [43], zinc oxide [38] silicon/silica/quartz [44–46], graphene oxide [47] have been used but other substrates like carbon nanotubes [48], cellulose
[49] or synthetic polymers [27] are also popular. The following major strategies for production of the polymer brushes systems were estab- lished: physical adsorption [50], chemical “grafting to” [42], “grafting from” [25] and “grafting through” [51] methods (see Fig. 1).
Physical adsorption method employs typically hydrogen bonds, van der Waals, or electrostatic interactions. It is a reversible process involving the self-assembly of macromolecules having appropriate blocks of functional groups interacting with the groups on the surface. Thermodynamically controlled equilibrium is of key importance for reaching high density of polymer brushes obtained using this method but in some cases the kinetic aspects are equally important [52]. The “grafting to” method is based on formation of stable bonds between the chain-end functional groups of the macromolecules and the properly modified substrate [53]. Unfortunately, this easy and straightforward method cannot lead to desired dense and thick brushes, mainly due to steric hindrance [54]. The “grafting from” method avoids those prob- lems due to gradual and simultaneous growth of the chains initiated from the surface-attached active centres (radical, ions etc.). It allows for precisely controlled grafting density and length of surface-grafted polymer chains so it is a widely used strategy for growing dense poly- mer brushes [55]. The “grafting through” strategy is a combination of
2

A.J. Wo´jcik et al.
European Polymer Journal 155 (2021) 110577
Fig. 1. Major strategies leading to fabrication of polymer brushes: a – physical adsorption of macromolecules, b – “grafting to”, c – “grafting from”, and d – “grafting through” methods.
the “grafting from” and “grafting to” methods because the process of creating chains of macromolecules occurs simultaneously in a solution and on a surface. Despite the simple synthetic procedure, it has some drawbacks which limit its widespread use. They include problems with controlling the thickness and density of the brushes, their relatively high roughness (dispersity of the chain lengths), as well as possible residues from the polymerization in the formed brushes [43].
The most common polymerizations used for grafting polymer brushes from surfaces are reversible-deactivation radical polymeriza- tions (RDRP) [56,57] that include: surface-initiated atom transfer radical polymerization (SI-ATRP), surface-initiated reversible-addition fragmentation chain transfer (SI-RAFT) polymerization, surface- initiated nitroxide-mediated radical polymerization (SI-NMP), and surface-initiated photoiniferter-mediated polymerization (SI-PMP or SI- PIMP). Besides RDRP techniques there are few other methods [58] like surface-initiated ring opening metathesis polymerization (SI-ROMP), surface-initiated ionic polymerizations [59], surface-initiated Suzuki, and Yamamoto polycondensation, Diels–Alder ligation [60], surface- initiated Kumada catalyst-transfer polycondensation (SI-KCTP) that are less versatile, and used typically for specific monomers only.
SI-ATRP as the most popular controlled surface-initiated polymeri-
zation method has been developing for the last two decades leading to numerous variants with e.g. better tolerance to the presence of oxygen or application of only trace amounts of metal complexes used as cata- lytic systems [61,62]. SI-ATRP owes its popularity not only to a well- controlled mechanism, but also to a relatively simple procedure of its practical implementation and commercial availability of reaction com- ponents. SI-ATRP enable synthesis of well-ordered, thick, dense brushes with advanced architectures such as: block copolymer, binary mixed, gradient brushes, etc. Besides, large tolerance to various functional groups, SI-ATRP is less efficient in polymerization of monomers bearing,
e.g. pyridine or carboxyl groups that can interact with metal (mainly copper) ions applied in the ATRP catalytic systems. Such controlled radical polymerizations cannot be also applied directly for fabrication of conjugated polymer brushes, which are highly demanded systems due to their electrical conductivity.
In 1972, M. Kumada and coworkers reported on the cross-coupling reactions of Grignard reagents and organic halides, which were cata- lyzed by nickel-phospine complexes [63]. In the next decades, these reactions were used in novel polymerization procedures leading to for- mation of conjugated polymers, namely, polythiophenes [64]. A usage of KCTP for the formation of conjugated polymer brushes via surface- initiated strategy was firstly reported by Senkovskyy and co-workers in 2007 [17] followed by other works [19,65]. Despite the fact, that SI-KCTP provides a good control over brush thickness (up to 120 nm thick poly(3-methylthiophene) brushes on ITO [66]), and it can be used for grafting brushes from many types of substrates, like gold, Si, ITO, organosilica microparticles and nanotubes [67], it still has some disad- vantages. First of all, it is characterized by a relatively low tolerance of the catalyst and initiator moieties to oxygen and humidity. That problem significantly complicates surface modification demanding very pure reagents and often low temperatures during the whole polymerization process [17]. The methodology limits also the number of potential monomer structures and substrates (to these being reactive towards Grignard reagents) [43,68,69]. It is worth emphasizing that polymeri- zation of large monomers by means of SI-KCTP is hindered, due to the mechanism that is based on “walking” bulky metal-based catalyst [70].
Up to date, conditions of SI-KCTP are well-described for thiophene-
based monomers and Pd/Ni-based precatalysts, but still require further research for other monomers [18,71] or fabrication more so- phisticated polymer brush topologies.
3. Unconventional polymer brush topologies

There is a growing number of polymer topologies that have been entering into the polymer brushes area bringing also interesting prop- erties to such novel coatings. They include but are not limited to (see also Fig. 2 for examples) [72–74]:
double-stranded polymers [20,75];
ladder polymers [76];
gel-brushes [77];
3

A.J. Wo´jcik et al.
European Polymer Journal 155 (2021) 110577
Fig. 2. Selected types of novel polymer brush topologies: a – gel-brush polymer brushes, b – Y-shaped binary mixed polymer brush, c – V-shaped binary mixed polymer brush, d – double-stranded surface-grafted polymer brushes with ladder-like architecture, e – cyclic polymer brush.
Y-shaped binary mixed polymer brushes [78];
V-shaped mixed polymer brushes [79];
double-stranded polymer brushes with ladder-like architecture
[43,80];
cyclic polymer brushes [28,29].
Conventional linear polymer brushes have been already recognized as very versatile functional nanocoatings for bio-related application
[81] such as fabrication of antifouling and proadhesive surfaces [82], antimicrobial coatings [83], in biomolecular separation techniques [84], bioelectronics [85], bioimaging [86]. They were also designed for applications in e.g., photovoltaic and energy storage systems [87], electromechanical systems [88], and optoelectronic devices [89]. However, novel polymer brush topologies may bring desired nano- mechanical [90], lubricating [91], optical [92] or conductive [93] properties that are hardly achievable in classical brushes and can significantly broaden the scope of their applications. Such demanding topologies drive also research on more versatile synthetic approaches that would enable obtaining of complex polymer brush systems.
Fig. 3. Schematic drawing of the surface-grafted ladder-type polymer brushes with conjugated chains that may serve as directional pathways for electron transport. Reprinted from Ref. [30] with permission from The Royal Society of Chemistry.

Obtaining polymer brushes with such unusual architecture (espe- cially with conjugated polymer chains) was made possible thanks to a novel strategy called self-templating surface-initiated polymerization (ST-SIP). The proposed approach is based on a sequence of two orthogonal polymerizations of a bifunctional monomer. One functional group of the monomer, e.g. methacryloyl one, is responsible for the formation of a template multimonomer chain in the first polymerization process. The second group (after deprotection if necessary), e.g. alkyne, thiophene or ethynylpyridine derivative, takes part in the formation of the second chain of a ladder (self-templating). Some examples of the applied bifunctional monomers that can lead to the formation of con- jugated chains are presented in Fig. 4.
Importantly, the template chains having pendant polymerizable groups (multimonomer chain) can be synthesized using facile SI-RDRP methods while the second polymerization can be selected for a given
3.1. Synthesis of double-stranded polymer brushes with ladder-like architecture
The double-stranded polymer brush with ladder-like structure is an example of unconventional topology which is in the focus of this paper. It was introduced in 2012 [30] in response to high interest in obtaining conjugated polymer brushes that cannot be easily synthesized using facile and common SI-RDRP methods. Such systems comprise two macromolecular chains connected with each other by molecular bridges, which resemble rungs of a ladder (Fig. 2d). In the originally obtained double-stranded systems only one strand of the pair was attached to the surface and number of chains were actually bridged intermolecularly leading to ladder-like rather than purely ladder brushes (Fig. 3). One of the strand was also a conjugated chain while in general any type of chains can be formed.
4

A.J. Wo´jcik et al.
European Polymer Journal 155 (2021) 110577

bridging the coils but not formation of ladder structures.
Nevertheless, the design of the bifunctional monomers has to take into account not only orthogonality of the planned polymerizations that may be ensured by chemical protection of the group reacting in the second process. The linker length, chain flexibility that can affect the constrains during formation of the second strand in the double-stranded brushes should be also tailored. The molecular size of a monomer may also limit the polymerization rate due to sterical hindrance so the structure has to be carefully adjusted to fulfil all the requirements.
In this first report [30] a bifunctional monomer, 3-trimethylsilyl-2- propynyl methacrylate (TPM), was grafted from gold surface. A controlled photopolymerization, SI-PMP, was used in the first step (Fig. 5a and b). After deprotection (Fig. 5c), the pendant acetylene groups were polymerized using rhodium-based catalyst leading to con- jugated polyacetylene chains (Fig. 5d), which were subsequently doped with iodine (Fig. 5e). This way, conductive polymer brushes were formed as confirmed using conductive atomic force microscopy (AFM) mapping.
The ST-SIP approach was later applied to other systems for which the first polymerization in a sequence was either SI-PMP [30,90,93,94] or SI-ATRP [80], while the second one – via rhodium-catalyzed coordina- tion polymerization [30], a catalyst-free quaternization polymerization (QP) [93] or oxidative polymerization with FeCl3 [43,80]. Instead of second polymerization, one may also consider modification of the pendant groups e.g. by click reaction introducing new functionality to the brushes [92].
Fig. 4. Structures of bifunctional monomers: green – functional group responsible for forming a template polymer chain in the first polymerization process, red – functional group used for formation of the second (conjugated) chain of a ladder, black – “linker” between two functional groups.

pendant group. This approach enables formation of high grafting density layers on various substrates, with precise control on the thickness and spatial arrangements offered by SI-RDRP methods. The second poly- merization benefits from the prearrangement of the polymerizable groups along the template chains adopting stretched conformation typical for polymer brushes. This is a crucial feature of the proposed approach as polymerization of multimonomer chains in solution would lead just to chemical crosslinking of the random coil they form and/or
Fig. 5. Scheme of synthesis of conductive brushes: (a) surface-initiated photopolymerization (SI-PMP) of TPM monomer, (b) a poly(TPM) brush, (c) deprotected template multimonomer brushes, (d) ladder-like brushes with conjugated polyacetylene chains, (e) doped conductive brushes.
5

A.J. Wo´jcik et al.

Application of the catalyst-free quaternization polymerization of ethynylpyridine-based multimonomers led to particularly interesting systems with charge linkers between the conjugated and nonconjugated chains in the ladders (Fig. 6) [93]. Unlike many polymerization pro- tocols that require penetration of the template brushes with bulky catalyst or oxidizing agents down to the grafting surface, the quaterni- zation polymerization proceed thanks to activation of the acetylene groups connected to the quaternized pyridine groups.
European Polymer Journal 155 (2021) 110577

applied solvent and in a dry state. Importantly, the controlled degrafting performed for the ladder-like brushes indicated that ca. ¼ of the mac- romolecules were not involved in intermolecular bridging during ST-SIP thus leading to formation of some isolated double-stranded structures.
In case of linear brushes, the swelling-induced degrafting process was observed for both hydrophilic [95] and hydrophobic [96] polymers attached to gold [97] or silicon oxide surface [98]. Wang et al. showed that high swelling ratio is the main factor that promotes hydrolytic cleavage of bonds at the brush-substrate interface [96]. Both the intra- and intermolecular bridges, which limit swelling of the brushes, seem to stabilize their surface-tethering as indicated by much higher resistance of the ladder-like poly(TPM) compared to linear parent poly(TPM) brushes to treatment with a tetrabutylammonium fluoride degrafting agent [90]. Nevertheless, incorporation of other structural motifs (e.g. hydrophobic blocks, hydrophobized initiators attached to the surface) [99–101] can be used to further enhance stability of the brushes by protecting the anchoring bonds against hydrolysis in an aqueous me- dium or humid environment. However, such methods should be tailored for conductive brushes as they may break the connections between the conjugated chains and the conductive substrate. In the case of double- stranded brushes a significant improvement in their stability could be
3.2. Properties of ladder-like polymer brushes

Polymer brushes with the ladder-like architecture exhibit interesting nanomechanical properties related to their specific double-stranded structure that limits the conformational freedom of polymer chains. It was shown, using AFM nanoindentation measurements, that such brushes with conjugated polyacetylene strands, exhibited enhanced stiffness and elastic response compared to the parent single-stranded brushes, in spite of lower layer density and more open (porous) struc- ture [90]. The studied brushes exhibited also very much limited swelling in good solvents, compared to parent brushes, indicating that they can keep their stretched conformation disregarding the quality of the
Fig. 6. ST-SIP strategy on an example of the synthesis of ladder-like conductive ionic PMTEP polymer brushes: A – surface-initiated photoiniferter-mediated polymerization of the MTEP monomer, B – multimonomer with protected acetylene groups, C – deprotection step, D – template polymerization and formation of ladder-like ionic brushes with polyacetylene chains, E – iodine doped conductive ionic polymer brushes. Reprinted from Ref. [93] with permission from the Royal Society of Chemistry.
6

A.J. Wo´jcik et al.

achieved by forming a covalent anchor between the second chain in a pair and the substrate that is still a challenge. Connecting covalently the conjugated chain in such brushes would also improve the out-of-plain conductivity, which is affected by the electrical resistance of such connection.
Moreover, the described topology plays an important role in providing a stable scaffold for conjugated chains to facilitate a direc- tional transport of charge carriers along those chains arranged normally to the surface and enhance their photo and thermal stability [94]. Such supported conjugated chains in the ladder-like structures were shown to sustain their electrical conductance for a long time storage even at ambient conditions, which are typically destructive for single-stranded doped conjugated chains. Thus, they seem to be much less susceptible to degradation and/or oxidation thanks to the presence of the support- ing unconjugated chain. Furthermore, it was shown that the higher the grafting density of the brushes the higher the stability of the formed polyacetylene chains – most likely due to less conformational freedom and higher stretching of surface-grafted chains [94].
Similar trend concerning photo- and air-stability of conjugated
brushes was revealed for a double-stranded poly(3-methylthienyl methacrylate) brushes [80]. Additionally, fabrication of the brushes with higher grafting density resulted in polythiophene chains with longer effective conjugation length, which was found also to scale with the brush thickness. As a result the effective conjugation length as long as 90–100 mers was evidenced for 80 nm thick brushes as determined by UV–Vis spectroscopy.
Introduction of charged groups into the conjugated ladder-like structure helped to achieve even more desired structures resulting in very high conductance of the brushes in the direction perpendicular to the grafting surface [93]. The synthesized doped brushes composed of
the ethynylpyridine-based monomer (PMTEP) showed directional con- ductivity as high as 10-2 S/cm indicating long effective conjugation length. While some connections between the neighboring chains may be
formed during the second polymerization, they seemed not to break the conjugation significantly as it was preserved in the system enabling efficient electron flow along the chain as shown using conductive/ tunnelling AFM (Fig. 7).
The mentioned above properties of the conjugated brushes with ladder-like architecture are crucial for their potential application in photovoltaic and optoelectronic devices where directional and high conductance are required together with good processability and long term stability.
Detailed physicochemical and structural characterization of the ladder-like polymer brushes requires applications of adequate methods. UV–Vis spectroscopy measurements were used to determine effective conjugation length of polymer brushes [43,80]. Combination of FTIR grazing angle spectroscopy and AFM enabled revealing how the orien- tation of polymer chains affects conductivity of the brushes [80]. Conductive AFM [30], tunnelling AFM (tuna-AFM) [93] mapping and current-voltage measurements were used for quantitative analysis of electrical properties of polymer brushes as macroscopic out-of-plane conductivity measurements of such thin films are problematic [102]. AFM quantitative nanomechanical mapping enabled simultaneous mapping of morphology and stiffness (i.e. Young’s modulus) of the brush samples while XPS was commonly used to follow the course of the sequence reaction as well as further oxidation/degradation of the brushes.
3.3. Perspective of polymer brushes with ladder-like architecture

The presented brushes with novel ladder-like architecture have an application potential primarily related to the possibility of formation conjugated (semiconductive or conductive) chains arranged perpen- dicularly to the grafting surface. Such molecular wires with highly anisotropic electrical conductivity (mainly in vertical direction) would be ideal components of the ultimate solar cell architecture (Fig. 8c)
European Polymer Journal 155 (2021) 110577
Fig. 7. Conductive AFM mapping of the doped PMTEP brush grafted from ITO surface: (A) topography image, (B) current map at 25 mV DC sample bias, (C) adhesion map. Reprinted from Ref. [93] with permission from the Royal Society of Chemistry.

[103]. Combination of polymer brushes with electron and hole con- ducting characteristics in the ordered heterojunction morphology would ensure good interfacial contact and short paths for the transporting charges that would limiting their loss and lead to superior energy con- version efficiency.
The covalently tethered and regularly arranged conjugated brushes would be also of high interest for construction of nanoelectronic, opto- electronic, biosensor, light-harvesting devices, which demand controlled transport of charges or excitons on the nanometer scale. Further development of flexible solar cells [104] as well as electro- chemical supercapacitors [105] also needs highly flexible and conduc- tive electrodes that can be fabricated by grafting conductive brushes from respective surfaces.
Conductive and elastic thin layers are also desired biointerface for studying e.g. mechanobiology, influence of electrical and mechanical stimuli on cell adhesion and proliferation [106]. While conductive polymers are generally considered to be biocompatible, the respective polymer brushes may be further modified, especially with the double- stranded topology, to improve their bioapplicability. Conductive brushes may not only transduce the chemical signal into an easily readable electrical one (biosensors) but also deliver electrical stimula- tion to cells to control their growth or differentiation (scaffolds) [107]. The directional charge flow offered by conductive brushes is of high interest for neuronal interfacing and stimulation, a rapidly developing part of regenerative medicine [108]. Conductive brushes have not been yet broadly explored in the abovementioned bioapplications mainly due to synthetic limitations but the versatility of the ST-SIP may pave the way for their more common applications in tailoring biointerfaces.
7

A.J. Wo´jcik et al.
European Polymer Journal 155 (2021) 110577
Fig. 8. Various architectures of organic solar cells: (a) planar bilayer morphology, (b) bulk heterojuncion morphology and (c) ordered heterojunction morphology.
4. Conclusions

In addition to the classical single-stranded linear polymer brushes, other, more complex brush topologies have been recently introduced. One of them is the double-stranded polymer brushes with one strand being a conjugated macromolecule. Such systems were formed using self-templating surface-initiated polymerization (ST-SIP) approach that is based on a sequential polymerization of a bifunctional monomer. This way, ladder-like brushes could be fabricated using facile controlled radical polymerizations in the first step and other types of polymeriza- tions in the second step producing conjugated strands, which are bridged with the previously formed unconjugated template chains.
This versatile methodology was developed in response to high de- mand for conjugated polymer brushes, which can provide directional transport of charges at the nanoscale that is crucial for potential appli- cations in photovoltaics, optoelectronics, fabrication of nanosensors or energy storage devices. ST-SIP was applied to form ladder-like brushes
containing polyacetylene, polythiophene and polyethynylpyridine con- jugated chains arranged normally to the grafting surface and exhibiting electrical conductivity as high as 10-2 S/cm. It was also shown that
thanks to this topology, the conjugated chains exhibited significantly enhanced photo and thermal stability compared to single stranded polymers. The nanomechanical characterization revealed that the ladder-like brushes exhibited enhanced stiffness and elastic response compared to the parent single-stranded brushes. The double-stranded structure, which limits the conformational freedom of polymer chains, was shown also to preserve their stretched conformation disregarding quality of the applied solvents, that is crucial for achieving long conju- gation length.
In summary, the double-stranded brush topology described here due to e.g. tunable and anisotropic conductance, unique nanomechanical characteristics, resistance to degrafting in various solvents, have high potential as robust nanocoating and (bio)interfaces of various func- tionalities defined by the component strands as well as post- polymerization modifications including doping and incorporation of various nanomaterials in to the stiff but porous brushes.
CRediT authorship contribution statement
Artur J. Wo´jcik: Conceptualization, Writing - original draft. Karol Wolski: Conceptualization, Writing - original draft. Szczepan Zapo- toczny: . : Conceptualization, Writing - review & editing.

Declaration of Competing Interest

The authors declare that they have no known competing financial interests or personal relationships that could have appeared to influence the work reported in this paper.

Acknowledgements

This work was supported by TEAM programme (grant number TEAM/2016-1/9) of the Foundation for Polish Science cofinanced by the
European Union under the European Regional Development Fund. The authors would like to kindly thank Lizaveta Fiadosava-Wo´jcik for creating some graphics.

References
1. Z. Li, C.-C. Chueh, A.K.-Y. Jen, Recent advances in molecular design of functional conjugated polymers for high-performance polymer solar cells, Prog. Polym. Sci. 99 (2019), 101175, https://doi.org/10.1016/j.progpolymsci.2019.101175.
2. N. Maity, A. Dawn, Conducting polymer grafting: recent and key developments, Polymers 12 (2020) 709, https://doi.org/10.3390/polym12030709.
3. Z. Qiu, B.A.G. Hammer, K. Müllen, Conjugated polymers – problems and promises, Prog. Polym. Sci. 100 (2020), 101179, https://doi.org/10.1016/j. progpolymsci.2019.101179.
4. S. Inal, J. Rivnay, A.-O. Suiu, G.G. Malliaras, I. McCulloch, Conjugated polymers in bioelectronics, Acc. Chem. Res. 51 (2018) 1368–1376, https://doi.org/ 10.1021/acs.accounts.7b00624.
5. R.B. Pernites, C.M. Santos, M. Maldonado, R.R. Ponnapati, D.F. Rodrigues, R.
C. Advincula, Tunable protein and bacterial cell adsorption on colloidally templated superhydrophobic polythiophene films, Chem. Mater. 24 (2012) 870–880, https://doi.org/10.1021/cm2007044.
1. M.M. Potter, D. Guironnet, Photophysical properties of soluble light-harvesting polyhydrofurans from post-polymerization functionalization of polyketones, Eur. Polym. J. 147 (2021), 110302, https://doi.org/10.1016/j. eurpolymj.2021.110302.
2. L. Luo, W. Huang, C. Yang, J. Zhang, Q. Zhang, Recent advances on π-conjugated
polymers as active elements in high performance organic field-effect transistors, Front. Phys. 16 (2021) 33500, https://doi.org/10.1007/s11467-020-1045-6.
1. A.R. Murad, A. Iraqi, S.B. Aziz, S.N. Abdullah, M.A. Brza, Conducting polymers for optoelectronic devices and organic solar cells: a review, Polymers 12 (2020) 2627, https://doi.org/10.3390/polym12112627.
2. P. Bujak, I. Kulszewicz-Bajer, M. Zagorska, V. Maurel, I. Wielgus, A. Pron´, Polymers for electronics and spintronics, Chem. Soc. Rev. 42 (2013) 8895–8999, https://doi.org/10.1039/C3CS60257E.
3. G. Zotti, B. Vercelli, A. Berlin, Monolayers and multilayers of conjugated polymers as nanosized electronic components, Acc. Chem. Res. 41 (2008) 1098–1109, https://doi.org/10.1021/ar8000102.
4. S. Fratini, M. Nikolka, A. Salleo, G. Schweicher, H. Sirringhaus, Charge transport in high-mobility conjugated polymers and molecular semiconductors, Nat. Mater. 19 (2020) 491–502, https://doi.org/10.1038/s41563-020-0647-2.
5. K. Wolski, M. Szuwarzyn´ski, M. Kope´c, S. Zapotoczny, Ordered photo- and
electroactive thin polymer layers, Eur. Polym. J. 65 (2015) 155–170, https://doi. org/10.1016/j.eurpolymj.2015.01.031.
1. S. Prodhan, J. Qiu, M. Ricci, O.M. Roscioni, L. Wang, D. Beljonne, Design rules to maximize charge-carrier mobility along conjugated polymer chains, J. Phys. Chem. Lett. 11 (2020) 6519–6525, https://doi.org/10.1021/acs.jpclett.0c01793.
2. E. Collini, G.D. Scholes, Coherent intrachain energy migration in a conjugated polymer at room temperature, Science 323 (2009) 369–373, https://doi.org/ 10.1126/science.1164016.
3. A. Bousquet, H. Awada, R.C. Hiorns, C. Dagron-Lartigau, L. Billon, Conjugated- polymer grafting on inorganic and organic substrates: a new trend in organic electronic materials, Prog. Polym. Sci. 39 (2014) 1847–1877, https://doi.org/ 10.1016/j.progpolymsci.2014.03.003.
4. J.O. Zoppe, N.C. Ataman, P. Mocny, J. Wang, J. Moraes, H.A. Klok, Surface- initiated controlled radical polymerization: state-of-the-art, opportunities, and challenges in surface and interface engineering with polymer brushes, Chem. Rev. 117 (2017) 1105–1318, https://doi.org/10.1021/acs.chemrev.6b00314.
5. V. Senkovskyy, N. Khanduyeva, H. Komber, U. Oertel, M. Stamm, D. Kuckling,
A. Kiriy, Conductive polymer brushes of regioregular head-to-tail poly(3- alkylthiophenes) via catalyst-transfer surface-initiated polycondensation, J. Am. Chem. Soc. 129 (2007) 6626–6632, https://doi.org/10.1021/ja0710306.
1. V. Senkovskyy, I. Senkovska, A. Kiriy, Surface-initiated synthesis of conjugated microporous polymers: chain-growth Kumada catalyst-transfer polycondensation at work, ACS Macro Lett. 1 (2012) 494–498, https://doi.org/10.1021/ mz200204g.
2. R. Tkachov, V. Senkovskyy, U. Oertel, A. Synytska, M. Horecha, A. Kiriy, Microparticle-supported conjugated polyelectrolyte brushes prepared by surface- initiated Kumada catalyst transfer polycondensation for sensor applications,
8

A.J. Wo´jcik et al.

Macromol. Rapid Commun. 31 (2010) 2146–2150, https://doi.org/10.1002/ marc.201000411.
  1. R.S.R.G. Jones, E.S. Wilks, M. Hess, T. Kitayama, W.V. Metanomski, Compendium of Polymer Terminology and Nomenclature IUPAC Recommendations 2008, The Royal Society of Chemistry, Cambridge, UK, 2008.
  2. J. Lee, A.J. Kalin, T. Yuan, M. Al-Hashimi, L. Fang, Fully conjugated ladder polymers, Chem. Sci. 8 (2017) 2503–2521, https://doi.org/10.1039/ C7SC00154A.
  3. Y.C. Teo, H.W.H. Lai, Y. Xia, Synthesis of ladder polymers: developments, challenges, and opportunities, Chem. Eur. J. 23 (2017) 14101–14112, https:// doi.org/10.1002/chem.201702219.
  4. J.-S. Wu, S.-W. Cheng, Y.-J. Cheng, C.-S. Hsu, Donor–acceptor conjugated polymers based on multifused ladder-type arenes for organic solar cells, Chem. Soc. Rev. 44 (2015) 1113–1154, https://doi.org/10.1039/C4CS00250D.
  5. W.J. Brittain, S. Minko, A structural definition of polymer brushes, J. Polym. Sci. Part A Polym. Chem. 45 (2007) 3505–3512, https://doi.org/10.1002/ pola.22180.
  6. S. Zapotoczny, Surface-grafted polymer brushes, in: A. Taubert, J.F. Mano, J.
C. Rodríguez-Cabello (Eds.), Biomaterials Surface Science, Wiley-VCH Verlag GmbH & Co. KGaA, Weinheim, 2013, pp. 27–43, https://doi.org/10.1002/ 9783527649600.ch2.
  1. P. Polanowski, J.K. Jeszka, K. Matyjaszewski, Polymer brushes in pores by ATRP: Monte Carlo simulations, Polymer 211 (2020), 123124, https://doi.org/10.1016/ j.polymer.2020.123124.
  2. X. Wang, N.S. Yadavalli, A.M. Laradji, S. Minko, Grafting through method for implanting of lysozyme enzyme in molecular brush for improved biocatalytic activity and thermal stability, Macromolecules 51 (2018) 5039–5047, https:// doi.org/10.1021/acs.macromol.8b00991.
  3. E.M. Benetti, M. Divandari, S.N. Ramakrishna, G. Morgese, W. Yan, L. Trachsel, Loops and cycles at surfaces: the unique properties of topological polymer brushes, Chem. Eur. J. 23 (2017) 12433–12442, https://doi.org/10.1002/ chem.201701940.
  4. G. Morgese, L. Trachsel, M. Romio, M. Divandari, S.N. Ramakrishna, E.M. Benetti, Topological polymer chemistry enters surface science: linear versus cyclic polymer brushes, Angew. Chem. Int. Ed. 55 (2016) 15583–15588, https://doi. org/10.1002/anie.201607309.
  5. M. Szuwarzyn´ski, J. Kowal, S. Zapotoczny, Self-templating surface-initiated
polymerization: a route to synthesize conductive brushes, J. Mater. Chem. 22 (2012) 20179–20181, https://doi.org/10.1039/c2jm34480g.
  1. P.G. de Gennes, Scaling theory of polymer adsorption, J. Phys. France 37 (1976) 1445–1452, https://doi.org/10.1051/jphys:0197600370120144500.
  2. S. Alexander, Adsorption of chain molecules with a polar head a scaling description, J. Phys. France 38 (1977) 983–987, https://doi.org/10.1051/jphys: 01977003808098300.
  3. A.A. Polotsky, T. Gillich, O.V. Borisov, F.A.M. Leermakers, M. Textor, T.
M. Birshtein, Dendritic versus linear polymer brushes: self-consistent field modeling, scaling theory, and experiments, Macromolecules 43 (2010) 9555–9566, https://doi.org/10.1021/ma101897x.
  1. C.M. Wijmans, E.B. Zhulina, G.J. Fleer, Effect of free polymer on the structure of a polymer brush and interaction between two polymer brushes, Macromolecules 27 (1994) 3238–3248, https://doi.org/10.1021/ma00090a017.
  2. K. Binder, A. Milchev, Polymer brushes on flat and curved surfaces: how computer simulations can help to test theories and to interpret experiments,
J. Polym. Sci. Part B Polym. Phys. 50 (2012) 1515–1555, https://doi.org/ 10.1002/polb.23168.
  1. P. Jungmann, T. Kreer, J.-U. Sommer, J. Paturej, Conformational properties of end-grafted bottlebrush polymers, Macromolecules 54 (2021) 161–169, https:// doi.org/10.1021/acs.macromol.0c01586.
  2. S.A. Egorov, H.-P. Hsu, A. Milchev, K. Binder, Semiflexible polymer brushes and the brush-mushroom crossover, Soft Matter 11 (2015) 2604–2616, https://doi. org/10.1039/C4SM02862G.
  3. A. Pomorska, K. Wolski, M. Wytrwał-Sarna, A. Bernasik, S. Zapotoczny, Polymer brushes grafted from nanostructured zinc oxide layers – spatially controlled decoration of nanorods, Eur. Polym. J. 112 (2019) 186–194, https://doi.org/ 10.1016/j.eurpolymj.2019.01.012.
  4. M. Szuwarzyn´ski, L. Zaraska, G.D. Sulka, S. Zapotoczny, Pulsatile releasing platform of nanocontainers equipped with thermally responsive polymeric nanovalves, Chem. Mater. 25 (2013) 514–520, https://doi.org/10.1021/ cm303930y.
  5. X. Sui, S. Zapotoczny, E.M. Benetti, M. Memesa, M.A. Hempenius, G.J. Vancso, Grafting mixed responsive brushes of poly(N-isopropylacrylamide) and poly (methacrylic acid) from gold by selective initiation, Polym. Chem. 2 (2011) 879–884, https://doi.org/10.1039/c0py00393j.
  6. J. Yan, X. Pan, Z. Wang, Z. Lu, Y. Wang, L. Liu, J. Zhang, C. Ho, M.R. Bockstaller,
K. Matyjaszewski, A fatty acid-inspired tetherable initiator for surface-initiated atom transfer radical polymerization, Chem. Mater. 29 (2017) 4963–4969, https://doi.org/10.1021/acs.chemmater.7b01338.
  1. M. Divandari, G. Morgese, S.N. Ramakrishna, E.M. Benetti, Surface-grafted assemblies of cyclic polymers: shifting between high friction and extreme lubricity, Eur. Polym. J. 110 (2019) 301–306, https://doi.org/10.1016/j. eurpolymj.2018.11.039.
  2. K. Wolski, A. Gruszkiewicz, S. Zapotoczny, Conductive polythiophene-based brushes grafted from an ITO surface via a self-templating approach, Polym. Chem. 6 (2015) 7505–7513, https://doi.org/10.1039/c5py01057h.
European Polymer Journal 155 (2021) 110577

1. A. Bali´s, K. Wolski, S. Zapotoczny, Thermoresponsive polymer gating system on mesoporous shells of silica particles serving as smart nanocontainers, Polymers 12 (2020) 888, https://doi.org/10.3390/POLYM12040888.
2. A.S. Schulz, H. Gojzewski, J. Huskens, W.L. Vos, G.J. Vancso, Controlled sub-10- nanometer poly(N-isopropyl-acrylamide) layers grafted from silicon by atom transfer radical polymerization, Polym. Adv. Technol. 29 (2018) 806–813, https://doi.org/10.1002/pat.4187.
3. M. Słowikowska, K. Chajec, A. Michalski, S. Zapotoczny, K. Wolski, Surface- initiated photoinduced iron-catalyzed atom transfer radical polymerization with ppm concentration of FeBr3 under visible light, Materials. 13 (2020) 5139, https://doi.org/10.3390/ma13225139.
4. M. Ilcikova, M. Galeziewska, M. Mrlik, J. Osicka, M. Masar, M. Slouf,
M. Maslowski, M. Kracalik, R. Pietrasik, J. Mosnacek, J. Pietrasik, The effect of short polystyrene brushes grafted from graphene oxide on the behavior of miscible PMMA/SAN blends, Polymer 211 (2020), 123088, https://doi.org/ 10.1016/j.polymer.2020.123088.
B. Ernould, M. Devos, J.P. Bourgeois, J. Rolland, A. Vlad, J.F. Gohy, Grafting of a redox polymer onto carbon nanotubes for high capacity battery materials,
J. Mater. Chem. A 3 (2015) 8832–8839, https://doi.org/10.1039/c5ta00570a.
1. R. Alosmanov, K. Wolski, S. Zapotoczny, Grafting of thermosensitive poly(N- isopropylacrylamide) from wet bacterial cellulose sheets to improve its swelling- drying ability, Cellulose 24 (2017) 285–293, https://doi.org/10.1007/s10570- 016-1120-x.
2. P. Brandani, P. Stroeve, Adsorption and desorption of PEO-PPO-PEO triblock copolymers on a self-assembled hydrophobic surface, Macromolecules 36 (2003) 9492–9501, https://doi.org/10.1021/ma0342675.
3. W. Choi, H. Sun, C. Battistella, O. Berger, M.A. Vratsanos, M.M. Wang, N.
C. Gianneschi, Biomolecular densely grafted brush polymers: oligonucleotides, oligosaccharides and oligopeptides, Angew. Chem. Int. Ed. 59 (2020) 19762–19772, https://doi.org/10.1002/anie.202005379.
1. K. Purohit, M. Mirville, S. Yang, A. Shukla, V. Chalivendra, Conductive nanobrush synthesized by physical grafting of conducting polymers on carbon nanotube, Mrsf10-1304-z09-02, MRS Proceedings 1304 (2011), https://doi.org/10.1557/ opl.2011.593.
2. A. Krywko-Cendrowska, S. di Leone, M. Bina, S. Yorulmaz-Avsar, C.G. Palivan,
W. Meier, Recent advances in hybrid biomimetic polymer-based films: from assembly to applications, Polymers 12 (2020) 1003, https://doi.org/10.3390/ POLYM12051003.
1. N. Ayres, Polymer brushes: applications in biomaterials and nanotechnology, Polym. Chem. 1 (2010) 769–777, https://doi.org/10.1039/b9py00246d.
2. W.-L. Chen, R. Cordero, H. Tran, C.K. Ober, 50th Anniversary perspective: polymer brushes: novel surfaces for future materials, Macromolecules 50 (2017) 4089–4113, https://doi.org/10.1021/acs.macromol.7b00450.
3. X. Pan, M.A. Tasdelen, J. Laun, T. Junkers, Y. Yagci, K. Matyjaszewski, Photomediated controlled radical polymerization, Prog. Polym. Sci. 62 (2016) 73–125, https://doi.org/10.1016/j.progpolymsci.2016.06.005.
4. A. Olivier, F. Meyer, J.-M. Raquez, P. Damman, P. Dubois, Surface-initiated controlled polymerization as a convenient method for designing functional polymer brushes: from self-assembled monolayers to patterned surfaces, Prog. Polym. Sci. 37 (2012) 157–181, https://doi.org/10.1016/j. progpolymsci.2011.06.002.
5. C.J. Reese, S.G. Boyes, New methods in polymer brush synthesis: Non-vinyl-based semiflexible and rigid-rod polymer brushes, Prog. Polym. Sci. 114 (2021), 101361, https://doi.org/10.1016/j.progpolymsci.2021.101361.
6. R. Advincula, Polymer brushes by anionic and cationic surface-initiated polymerization (SIP), Adv. Polym. Sci. 197 (2006) 107–136, https://doi.org/ 10.1007/12_066.
7. B. Yameen, C. Rodriguez-Emmenegger, C.M. Preuss, O. Pop-Georgievski,
E. Verveniotis, V. Trouillet, B. Rezek, C. Barner-Kowollik, A facile avenue to conductive polymer brushes via cyclopentadiene–maleimide Diels-Alder ligation, Chem. Commun. 49 (2013) 8623, https://doi.org/10.1039/c3cc44683b.
1. M.N. Nguyen, T. Matrab, C. Badre, M. Turmine, M.M. Chehim, Interfacial aspects of polymer brushes prepared on conductive substrates by aryl diazonium salt surface-initiated ATRP, Surf. Interface Anal. 40 (2008) 412–417, https://doi.org/ 10.1002/sia.2687.
2. J. Yan, M.R. Bockstaller, K. Matyjaszewski, Brush-modified materials: control of molecular architecture, assembly behavior, properties and applications, Prog. Polym. Sci. 100 (2020), 101180, https://doi.org/10.1016/j. progpolymsci.2019.101180.
3. K. Tamao, K. Sumitani, M. Kumada, Selective carbon-carbon bond formation by cross-coupling of Grignard reagents with organic halides. Catalysis by nickel- phosphine complexes, J. Am. Chem. Soc. 94 (1972) 4374–4376, https://doi.org/ 10.1021/ja00767a075.
4. R.S. Loewe, S.M. Khersonsky, R.D. McCullough, A simple method to prepare head-to-tail coupled, regioregular poly(3-alkylthiophenes) using Grignard metathesis, Adv. Mater. 11 (1999) 250–253, https://doi.org/10.1002/(SICI)
1521-4095(199903)11:3<250::AID-ADMA250>3.0.CO;2-J.
1. L. Yang, S.K. Sontag, T.W. Lajoie, W. Li, N.E. Huddleston, J. Locklin, W. You, Surface-initiated poly(3-methylthiophene) as a hole-transport layer for polymer solar cells with high performance, ACS Appl. Mater. Interfaces. 4 (2012) 5069–5073, https://doi.org/10.1021/am301401n.
2. I.A. Vonwald, M.M. Moog, T.W. Lajoie, J.D. Yablonski, D.M. Delongchamp,
J. Locklin, F. Tsui, W. You, Morphology, structure, and enhanced intramolecular conduction in ultralong conjugated polymer brushes, J. Phys. Chem. C 122 (2018) 7586–7596, https://doi.org/10.1021/acs.jpcc.8b00033.
9

A.J. Wo´jcik et al.

  1. M. Alonzi, D. Lanari, A. Marrocchi, Ch. Petrucci, L. Vaccaro, Synthesis of polymeric semiconductors by a surface-initiated approach, RSC Adv. 3 (2013) 23909–23923, https://doi.org/10.1039/C3RA43680B.
  2. C. Horn, D. Pospiech, J. Zessin, S. Stein, D. Jehnichen, H. Komber, M. Go¨bel,
B. Voit, A. Kiriy, Synthesis and characterization of a regioregular side-chain semifluorinated polythiophene, Polythiophene 216 (2019) 1800747, https://doi. org/10.1002/pssa.201800747.
  1. A. Kiriy, V. Senkovskyy, M. Sommer, Kumada catalyst-transfer polycondensation: mechanism, opportunities, and challenges, Macromol. Rapid Commun. 32 (2011) 1503–1517, https://doi.org/10.1002/marc.201100316.
  2. R. Tkachov, V. Senkovskyy, H. Komber, J.-U. Sommer, A. Kiriy, Random catalyst walking along polymerized poly(3-hexylthiophene) chains in Kumada catalyst- transfer polycondensation, J. Am. Chem. Soc. 132 (2010) 7803–7810, https:// doi.org/10.1021/ja102210r.
  3. T. Erdmann, J. Back, R. Tkachov, A. Ruff, B. Voit, S. Ludwigs, A. Kiriy, Dithienosilole-based all-conjugated block copolymers synthesized by a combination of quasiliving Kumada and Negishi catalyst-transfer polycondensations, Polym. Chem. 5 (2014) 5383–5390, https://doi.org/ 10.1039/C4PY00747F.
  4. N. Khanduyeva, V. Senkovskyy, T. Beryozkina, M. Horecha, M. Stamm, C. Uhrieh,
M. Riede, K. Leo, A. Kiriy, Surface engineering using Kumada catalyst-transfer polycondensation (KCTP): preparation and structuring of poly(3- hexylthiophene)-based graft copolymer brushes, J. Am. Chem. Soc. 131 (2009) 153–161, https://doi.org/10.1021/ja8050734.
  1. W. Kim, J. Jung, Polymer brush: a promising grafting approach to scaffolds for tissue engineering, BMB Rep. 49 (2016) 655–661, https://doi.org/10.5483/ BMBRep.2016.49.12.166.
  2. B. Zhao, W.J. Brittain, Polymer brushes: surface-immobilized macromolecules, Prog. Polym. Sci. 25 (2000) 677–710, https://doi.org/10.1016/S0079-6700(00) 00012-5.
  3. E. Yashima, K. Maeda, Y. Furusho, Single- and double-stranded helical polymers: synthesis, structures, and functions, Acc. Chem. Res. 41 (2008) 1166–1180, https://doi.org/10.1021/ar800091w.
  4. C. Zhu, A.J. Kalin, L. Fang, Covalent and noncovalent approaches to rigid coplanar π-conjugated molecules and macromolecules, Acc. Chem. Res. 52 (2019) 1089–1100, https://doi.org/10.1021/acs.accounts.9b00022.
  5. E.M. Benetti, X. Sui, S. Zapotoczny, G. Julius Vancso, Surface-grafted gel-brush/ metal nanoparticle hybrids, Adv. Funct. Mater. 20 (2010) 939–944, https://doi. org/10.1002/adfm.200902114.
  6. D. Julthongpiput, Y.-H. Lin, J. Teng, E.R. Zubarev, V.V. Tsukruk, Y-shaped polymer brushes: nanoscale switchable surfaces, Langmuir 19 (2003) 7832–7836, https://doi.org/10.1021/la035007j.
  7. W. Sun, S. Zhou, B. You, L. Wu, Polymer brush-functionalized surfaces with unique reversible double-stimulus responsive wettability, J. Mater. Chem. A 1 (2013) 10646–10654, https://doi.org/10.1039/C3TA12367G.
  8. K. Wolski, A. Gruszkiewicz, M. Wytrwał-Sarna, A. Bernasik, S. Zapotoczny, The grafting density and thickness of polythiophene-based brushes determine the orientation, conjugation length and stability of the grafted chains, Polym. Chem. 8 (2017) 6250–6262, https://doi.org/10.1039/c7py01418j.
  9. L. Moroni, M. Klein Gunnewiek, E.M. Benetti, Polymer brush coatings regulating cell behavior: passive interfaces turn into active, Acta Biomater. 10 (2014) 2367–2378, https://doi.org/10.1016/j.actbio.2014.02.048.
  10. I. Lilge, H. Scho¨nherr, Synthesis and characterization of well-defined ligand-
terminated block copolymer brushes for multifunctional biointerfaces, Polymer 98 (2016) 409–420, https://doi.org/10.1016/j.polymer.2016.03.031.
  1. G. Gao, K. Yu, J. Kindrachuk, D.E. Brooks, R.E.W. Hancock, J.N. Kizhakkedathu, Antibacterial surfaces based on polymer brushes: investigation on the influence of brush properties on antimicrobial peptide immobilization and antimicrobial activity, Biomacromolecules 12 (2011) 3715–3727, https://doi.org/10.1021/ bm2009697.
  2. K. Nagase, S. Ishii, K. Ikeda, S. Yamada, D. Ichikawa, A.M. Akimoto, Y. Hattori,
H. Kanazawa, Antibody drug separation using thermoresponsive anionic polymer brush modified beads with optimised electrostatic and hydrophobic interactions, Sci. Rep. 10 (2020) 1–13, https://doi.org/10.1038/s41598-020-68707-7.
  1. N. Wang, C. Wang, H. Chen, L. Bai, W. Wang, H. Yang, D. Wei, L. Yang, Facile fabrication of a controlled polymer brush-type functional nanoprobe for highly sensitive determination of alpha fetoprotein, Anal. Methods. 12 (2020) 4438–4446, https://doi.org/10.1039/d0ay01151g.
  2. B. Wang, B. Li, B. Dong, B. Zhao, C.Y. Li, Homo- and hetero-particle clusters formed by Janus nanoparticles with bicompartment polymer brushes, Macromolecules 43 (2010) 9234–9238, https://doi.org/10.1021/ma101772f.
  3. J.M. Giussi, M.L. Cortez, W.A. Marmisoll´e, O. Azzaroni, Practical use of polymer
brushes in sustainable energy applications: interfacial nanoarchitectonics for
European Polymer Journal 155 (2021) 110577

high-efficiency devices, Chem. Soc. Rev. 48 (2019) 814–849, https://doi.org/ 10.1039/C8CS00705E.
[88] P. Enrique-Jimenez, S. Quiles-Díaz, H.J. Salavagione, D. Wesner, H. Scho¨nherr,
J. Gonz´alez-Casablanca, R. García-Quismondo, G. Martínez, M.A. Go´mez-Fatou,
F. Ania, A. Flores, Control of the structure and properties of SEBS nanocomposites via chemical modification of graphene with polymer brushes, Eur. Polym. J. 97 (2017) 1–13, https://doi.org/10.1016/j.eurpolymj.2017.09.047.
1. S. Kang, R.J. Ono, C.W. Bielawski, Controlled catalyst transfer polycondensation and surface-initiated polymerization of a p-phenyleneethynylene-based monomer, J. Am. Chem. Soc. 135 (2013) 4984–4987, https://doi.org/10.1021/ ja401740m.
2. M. Słowikowska, K. Wolski, A.J. Wo´jcik, D. Wesner, H. Scho¨nherr, S. Zapotoczny, Unraveling the nanomechanical properties of surface-grafted conjugated polymer brushes with ladder-like architecture, Polym. Chem. 11 (2020) 7050–7062, https://doi.org/10.1039/d0py01422b.
3. E.M. Benetti, N.D. Spencer, Using polymers to impart lubricity and biopassivity to surfaces: are these properties linked? Helv. Chim. Acta 102 (2019), e1900071 https://doi.org/10.1002/hlca.201900071.
4. M. Szuwarzyn´ski, K. Wolski, A. Pomorska, T. Uchacz, A. Gut, Ł. Łapok,
S. Zapotoczny, Photoactive surface-grafted polymer brushes with phthalocyanine bridging groups as an advanced architecture for light-harvesting, Chem. – A Eur. J. 23 (2017) 11239–11243, https://doi.org/10.1002/chem.201702737.
1. K. Wolski, M. Szuwarzyn´ski, S. Zapotoczny, A facile route to electronically conductive polyelectrolyte brushes as platforms of molecular wires, Chem. Sci. 6 (2015) 1754–1760, https://doi.org/10.1039/c4sc04048a.
2. M. Szuwarzyn´ski, K. Wolski, S. Zapotoczny, Enhanced stability of conductive
polyacetylene in ladder-like surface-grafted brushes, Polym. Chem. 7 (2016) 5664–5670, https://doi.org/10.1039/c6py00977h.
1. M.B. P´erez, M. Cirelli, S. de Beer, Degrafting of polymer brushes by exposure to humid air, ACS Appl. Polym. Mater. 2 (2020) 3039–3043, https://doi.org/ 10.1021/acsapm.0c00474.
2. J. Wang, H.-A. Klok, Swelling-induced chain stretching enhances hydrolytic degrafting of hydrophobic polymer brushes in organic media, Angew. Chem. Int. Ed. 58 (2019) 9989–9993, https://doi.org/10.1002/anie.201904436.
3. Y. Zhang, B. Lv, Z. Lu, J. He, S. Zhang, H. Chen, H. Ma, Predicting Au–S bond breakage from the swelling behavior of surface tethered polyelectrolytes, Soft Matter 7 (2011) 11496–11500, https://doi.org/10.1039/C1SM05895A.
4. H.-A. Klok, J. Genzer, Expanding the polymer mechanochemistry toolbox through surface-initiated polymerization, ACS Macro Lett. 4 (2015) 636–639, https://doi. org/10.1021/acsmacrolett.5b00295.
5. R. Quintana, M. Gosa, D. Jan´czewski, E. Kutnyanszky, G.J. Vancso, Enhanced stability of low fouling zwitterionic polymer brushes in seawater with diblock architecture, Langmuir 29 (2013) 10859–10867, https://doi.org/10.1021/ la402287a.
[100]
D. Paripovic, H.-A. Klok, Improving the stability in aqueous media of polymer brushes grafted from silicon oxide substrates by surface-initiated atom transfer radical polymerization, Macromol. Chem. Phys. 212 (2011) 950–958, https://doi. org/10.1002/macp.201000729.
M. Divandari, E.S. Dehghani, N.D. Spencer, S.N. Ramakrishna, E.M. Benetti, Understanding the effect of hydrophobic protecting blocks on the stability and biopassivity of polymer brushes in aqueous environments: A Tiramisu for cell- culture applications, Polymer 98 (2016) 470–480, https://doi.org/10.1016/j. polymer.2016.04.042.
K. van de Ruit, I. Katsouras, D. Bollen, T. van Mol, R.A.J. Janssen, D.M. de Leeuw,
M. Kemerink, The curious out-of-plane conductivity of PEDOT:PSS, Adv. Funct. Mater. 23 (2013) 5787–5793, https://doi.org/10.1002/adfm.201301175.
J.T. Chen, C.S. Hsu, Conjugated polymer nanostructures for organic solar cell applications, Polym. Chem. 2 (2011) 2707, https://doi.org/10.1039/ C1PY00275A.
J. Zhang, W. Zhang, H.-M. Cheng, S.R.P. Silva, Critical review of recent progress of flexible perovskite solar cells, Mater. Today 39 (2020) 66–88, https://doi.org/ 10.1016/j.mattod.2020.05.002.
K.D. Fong, T. Wang, S.K. Smoukov, Multidimensional performance optimization of conducting polymer-based supercapacitor electrodes, Sustain. Energy Fuels 1 (2017) 1857–1874, https://doi.org/10.1039/C7SE00339K.
I. Bernardeschi, F. Greco, G. Ciofani, A. Marino, V. Mattoli, B. Mazzolai, L. Beccai, A soft, stretchable and conductive biointerface for cell mechanobiology, Biomed. Microdevices 17 (2015) 46, https://doi.org/10.1007/s10544-015-9950-0.
A.J. Hackett, J. Malmstro¨m, J. Travas-Sejdic, Functionalization of conducting polymers for biointerface applications, Progr. Polym. Sci. 70 (2017) 18–33, https://doi.org/10.1016/j.progpolymsci.2017.03.004.
Y. Wu, Q. Zhang, H. Wang, M. Wang, Multiscale engineering of functional organic polymer interfaces for neuronal stimulation and recording, Mater. Chem. Front. 4 (2020) 3444–3471, https://doi.org/10.1039/D0QM00279H.
[101]
[102]
[103]
[104]
[105]
[106]
[107]
[108]
10