Catal Lett (2016) 146:998–1010 DOI 10.1007/s10562-016-1716-7
Molybdenum Complexes as Catalysts for the Oxidation
of Cycloalkanes with MolecularOxygen
AnnaSzyman´ska1•WojciechNitek2•MarcinOszajca2•WiesławŁasocha1,2•
Katarzyna Pamin1•Jan Połtowicz1
Received: 23 January 2016 / Accepted: 12 February 2016 / Published online: 3 March 2016
©The Author(s) 2016. This article is published with open access at Springerlink.com
Abstract A group of new polymolybdates was synthe- sized and tested in the catalytic oxidation of cycloalkanes. Investigated compounds exhibit broad structural diversity including polymolybdates with isolated anionic clusters (0- dim), polymeric anions (1-dim), Mo–O layers (2-dim) as well as hexagonal and orthorhombic molybdenum oxides (3-dim). All studied molybdenum complexes were foundto be active in the reaction conditions yielding ketones and alcohols as main products. In the case of layered com- pounds (2-dim), dicarboxylic acid was detected in the mixture of reaction products. The structure of investigated molybdenum compounds was shown to have influence on yields and selectivities of the investigated reactions.Anionic layers separation (in 2-dim materials) as well as type and charge of organic cations present in the com- pounds are prime examples of structural factorsinfluencing the oxidation reactions efficiencies. On the basis of obtained results and literature reports a mechanism for the oxidation of cycloalkanes by polymolybdates has been proposed.
Graphical Abstract
Keywords Cycloalkanes oxidation·Heterogeneous catalysis·Polyoxometalates synthesis·X-ray diffraction·Single crystal·Powder diffraction
1 Introduction
Molybdenum complexes are well known as active centers of several enzymes such as oxotransferases [1–4]. Some molybdates show antiviral, antitumoral or antibiotic activity [5–7]. They are also known as efficient catalysts for the oxidation of various organic compounds with different oxygen donors like ROOH [8–20] and H2O2[21–29]. Molybdenum(VI) dioxo or oxodiperoxo compounds are commonly encountered in oxidation catalysis. It has been shown that mononuclear peroxo and mono-oxo bridged dinuclear molybdenum complexes are active cat- alysts for the epoxidation of olefins and nonfunctionalized olefins with t-butylhydroperoxide TBHP as oxygen donor [8,13–15]. The epoxidation of olefins catalyzed by a large family of complexes with MoO2X2(N–N)2or MoO2X2(N– O)2formula where N–N or N–O are bidenate ligands and X=Cl, Br or Me has been previously reported [10,11,15,16]. All these catalysts show high activity and selectivity.
Electronic supplementary material The online version of this article (doi:10.1007/s10562-016-1716-7) contains supplementary material, which is available to authorizedusers.
&
Wiesław Łasochalasocha@chemia.uj.edu.pl
1
Jerzy Haber Institute of Catalysis and Surface Chemistry PAS, Niezapominajek 8, 30-239 Krakow, Poland
Faculty of Chemistry, Jagiellonian University, Ingardena 3, 30-060 Krakow, Poland
2
13

Molybdenum Complexes as Catalysts for the Oxidation of Cycloalkanes with Molecular Oxygen
999
Molybdenum oxo-peroxo complexes were applied as catalysts for selective oxidation of arylalkyl, diaryl and dialkylsulfides to corresponding sulfoxides with TBHP as oxidant [30–33].
Recent studies have shown that oxo-peroxo molybde- num complexes in combination with H2O2can convert a wide range of hydrocarbons like alkanes and alkylbenzenes to the corresponding oxidized products [34]. Molybdenum oxo and oxo-peroxo complexes have been used for selec- tive oxidation of amines [13,30–33] and for oxidation of allylic alcohols with H2O2[34]. Dioxomolybdenum(VI) complexes with a N-salicylidene amino acid hydrazide[28] or oxazoline [16] ligand were applied for oxidation of sulfides with high selectivity to sulfoxides. Dioxomolyb-denum(VI)complexesoftheMoO2L2type(L=(20-piry-dyl)alcoholate) were used as catalysts for the selective terminal oxidation of n-alkanes with molecular oxygen [35]. The catalytic data indicate an important influence of ligand structure on the catalysts activity and product dis- tribution[35].
polyoxomolybdates of aromatic amines (three compounds of 4-methylaniline, six compounds of other aniline derivatives, two polyoxomolybdates of 4-methylpyridine). Five of them, namely: A3, B1, B2, B4 and C4 are new compounds, not previously reported. Consult Table1, for compounds description including chemical formulas, symbols used henceforward and graphical representations of their structures. Crystal structures of investigated cata- lysts, in particular new compounds, are described in chapter3.1.
Chemical syntheses of new compounds were carried out in aqueous solutions containing MoO3or molybdic acid and the appropriate amine. Full description of thesyntheses procedures, yields, results of chemical analyzes has been placed in Supporting Information(SI).
The details of X-ray diffraction experiments and resultsof crystal structure determination are also available in theSI. Crystal structures of A3 and B1 were studied by singlecrystal methods, other catalysts by ‘ab initio’ powderdiffraction methods. B2 and C4 were investigated with theuse of synchrotron radiation while B4 with a laboratorydiffractometer. Data concerning structure determinationand structure description are listed in Tables SI-1,2,3(single crystal data) SI-4,5,6,7 (powder data), structures aredepicted on accompanying Figs (SI-A3, B1, B2, B4, C4).While selecting catalysts, thermal stability data forprospective compounds were considered, and if reliabledata were not available temperature dependent XRPDstudies (in air, temp=25–600°C) were performed.Results are presented in SI. In general, all compounds werefound to be stable in reaction conditions and the mostactive compounds B1, B3, C2–C4 were stable up to
250°C.
Excluding samples obtained as large single crystals (A1–A3), surface areas for investigated samples were determined applying BET technique. Results of these experiments are presented in Table2.
Selected catalysts (B2, C2) after 6 h of reaction time were recovered by filtration, washed with propanol, driedin air, and reused in catalytic experiments. Obtained results arediscussedinchapter3(seealsoFig.3).
Selective catalytic molecular oxygen is
oxidation of cycloalkanes with one of the most importantand
attractive transformations in organic synthesis [36–38]. Itis evident that the use of molecular oxygen from air which is an inexpensive, abundant and readily available oxidant in place of other oxygen donors is clearly desirable on eco- nomic and environmental grounds.
Very recently, we have reported the synthesis, physico- chemical properties and catalytic activity of new oxodiperoxomolybdenum complexes with nicotinic acid in the oxidation of cyclooctane [39].
This paper is a result of combined studies on syntheses of new polymolybdate complexes together with research on their catalytic activity in cycloalkanes oxidation. Cat- alytic properties are discussed in relation to structural dimensionality of presented polyoxomolybdate complexes, various amounts and types of oxygen atoms (in terms of bonding arrangements) in their structures and ligands used insyntheses.
2 Experimental
3 Catalytic Investigation
2.1 Synthesis and Structural Characterization
For the purpose of this work, a group of 13 polyoxo- molybdenum compounds was selected. Three of them represent compounds with polyoxo moieties in the form of isolated clusters (denoted as An; n=1,2,3), 4 contain polymeric chains (Bn), we also investigated 4 layered compounds (Cn) and two ‘molybdenum oxides’. To determine the influence of structural features on catalytic activity, all selected compounds (except for MoO3) are
The liquid-phase oxidation of cycloalkanes (cyclopentane, cyclohexane or cyclooctane) was performed in a stainlees- steel batch reactor system at the optimum temperature of 393 K and under the pressure of 10 atm. with the reagents molar ratio CnH2n(where n=5, 6, 8):O2=13:2. A Te- flon-lined reactor of 1 L volume equipped with a magnetic stirrer was used. In a typical experiment, molybdenumbasedcatalysthavingtheconcentrationof3.3910-4M
13

Table 1 Basic parameters and structure drawings of the investigated Mo catalysts
Mo Catalyst. Dim-xa
Graphical representation of each group of investigated compoundsc. Colours denote: Mo—green, O—red, C—black, N—blue, H—small grey circlesd
Systematic name, reference if not new, moiety formula
Formula weight (g/mol), d(200)b
A1 0-dim
Tetrakis(4-methylpyridinium) bis(4-methylpyridine) c- octamolybdate hydrate, [43]
[Mo8O26·2(C6H7N)]·4(C6H7NH)·H2O
1764.32
A2 0-dim
Tetrakis(4-methylpyridinium)b-octamolybdate, [44] Mo8O26·4(C6H8N)
Tetrakis(4-methylanilinium) b-octamolybdate dihydrate Mo8O26·4(C6H4CH3NH3)·2H2O
1560.05
A3 0-dim
1652.19
B1 1-dim
1,2-phenylenediamine molybdenum oxide
MoO3(C6-H4(NH2)2)
252.08
A.Szyman´skaetal.
1000
13

Table 1 continued
Mo Catalyst. Dim-xa
Graphical representation of each group of investigated compoundsc. Colours denote: Mo—green, O—red, C—black, N—blue, H—small grey circlesd
Systematic name, reference if not new, moiety formula
Formula weight (g/mol), d(200)b
B2 1-dim
Bis(3,5-dimethylanilinium) trimolybdate Mo3O10·2(C6H3NH3(CH3)2)
692.19
B3 1-dim
1,3-phenylenediammonium trimolybdate, [45] Mo3O10·C6H4(NH3)2
Bis(4-methylanilinium) trimolybdate Mo3O10·2(CH3C6H4(NH3))
557.97
B4 1-dim
664.14
Molybdenum Complexes as Catalysts for the Oxidation of Cycloalkanes with Molecular Oxygen
1001
13

Table 1 continued
Mo Catalyst. Dim-xa
Graphical representation of each group of investigated compoundsc. Colours denote: Mo—green, O—red, C—black, N—blue, H—small grey circlesd
Systematic name, reference if not new, moiety formula
Formula weight (g/mol), d(200)b
923.96d(200)=13.60A˚
C1 2-dim
Bis(anilinium) pentamolybdate, [46] Mo5O162(NH3C6H5)
Bis(4-methylanilinium) pentamolybdate, [47] Mo5O16·2(C7H10N)
Bis(4-bromoanilium) pentamolybdate, [48] Mo5O16·2(NH3C6H4Br)
Bis(4-ethylanilinium) pentamolybdate Mo5O16·2(NH3C6H4C2H5)
952.02d(200)=14.36A˚
C2 2-dim
1081.76d(200)=14.81A˚
C3 2-dim
980.07d(200)=15.18A˚
C4 2-dim
D1 3-dim
Molybdenum trioxide, [49] MoO3(hexagonal)
143.94
D2 3-dim
Molybdenum trioxide, [50] MoO3(orthorhombic)
143.94
a
Dimensionality of the polyoxomolybdenum species Interlayerdistanceequald(200)forinvestigatedcompounds
The drawings of crystal structures were prepared using DIAMOND software [51]
Except for water molecules hydrogen atoms were omitted for clarity
b
c
d
A.Szyman´skaetal.
1002
13

Molybdenum Complexes as Catalysts for the Oxidation of Cycloalkanes with Molecular Oxygen
1003
Table 2 Cyclooctane oxidation with molecular oxygen and polyoxomolybdates as catalysts
Yield of ketonea(%) TONd
Yield of alcohola(%) TONd
Surface area m2/g
Mo catalyst
Ketone?alcohol(%)
Ketone/alcohol
A1A2A3B1 B2
B2bB3 B4
C1cC2cC3cC4cD1
D2
13.3
10.2
10.7
34.3
29.6
Traces 34.7
25.6
11.7
34.1
34.0
23.4
3.9
3.4
4990
3830
4010
12,860
11,100
–13,010
9600
4390
12,790
12,750
8780
1460
1280
9.3
4.4
9.4
16.6
15.5
Traces 13.6
15.9
5.5
10.8
10.6
15.3
2.7
2.4
3490
1650
3530
6230
5810
– 5100
5960
2060
4050
3975
5740
1010
900
22.6
14.6
20.1
50.9
45.1
– 48.3
41.5
17.2
44.9
44.6
38.7
6.6
5.8
1.4
2.3
1.1
2.1
1.9
–
2.6
1.6
2.1
3.2
3.1
1.5
1.4
1.4
4.56
2.91
12.47
9.59
4.34
1.91
4.66
3.76
a
Isolated yields calculated on the basis of oxygen quantity in batch reactor Reaction with free radical scavenger 2,6-di-tert-butyl-p-cresol
Suberic acid as by-product is observed (see Fig.4)
Molproduct9molcatalyst-19h-1
b
c
d
3.1
Catalysts Characterization—Crystal Structure Description
was introduced into the reaction mixture. The catalyst together with the substrate were closed in the air-free autoclave and were heated together with the whole system untiltemperatureof393Kwasreached.Induetimeairwas added to the hot reaction mixture in such amount that final pressure of 10 atm was obtained and the reaction started. After 6 h of reaction time the oxidation was stopped by immersing the hot reactor in a cold water bath. Reaction products (cycloketone and cycloalcohol) were analyzed by means of Agilent Technologies 6890 N gas chromatograph equipped with Innowax (30 m) column in the presence of chlorobenzene as internal standard. Amounts of CO and CO2were determined chromatographically using Perkin- Elmer Clarus 500 withmethanizer.
The amount of cycloalkane hydroperoxide in the reac- tion mixture was evaluated by the iodometric titration and Shul’pin method [40–42]. The yield of cycloalkylhydroperoxide(yield\0.1%)observedafter6hofthereaction is too small to have an impact on the results of the subsequent GC analysis.
Stability of catalysts in reaction conditions was tested in the following manner. Compounds B1 or C2 were mixed with cyclooctane and boiled (Tb=149°C) under reflux (in air) for 24 h. When the mixture was cooled down, catalysts were separated from cyclooctane by filtration and dried in air. Diffraction patterns and IR spectra of fresh catalysts and catalysts after cyclooctane treatment are presented in the Supporting Information (see Fig. SI-11,12 and Fig.SI-13,14).
Considering the structural diversity of presented poly- molybdates, in particular their dimensionality, the com- pounds were divided into four main categories. Octamolybdates A1–A3 contain isolated molybdenum- oxygen clusters (0-dim). Polymeric materials B1-B4 are built of infinite molybdenum-oxygen chains (1-dim). Compounds C1–C4 are formed by Mo–O layers with amines in between (2-dim). Two types of three-dimen- sional molybdenum trioxide D1 and D2 represent the last group of compounds (3-dim). The main subject of the presented research was to correlate catalytic activity with the structure of investigated polymolybdates. The number of terminal (oxo) and bridging oxygen atoms (ln) was also taken into account. In general, all investigated catalysts are Mo(VI) isopolyoxo compounds, with all Mo atoms in octahedral coordination surrounded only by oxygen or by oxygen and nitrogen atoms.
The basic parameters of the compounds with structure drawings are summarized in Table1. Main structural fea- tures are described below; data for new compounds are highlighted with bold font.
As representatives of isolated (0-dim) compounds we have selected c- and b-octamolybdates of 4-methylpyridine A1- A2, recently investigated by us [39]. Thesecompounds were supplemented by a new b-octamolybdate of 4-methylanilinium A3 obtained withinthis study.
13

A.Szyman´skaetal.
1004
CompoundsA1–A3arebuiltofisolatedoctamolybdate clusters (0-dim). Eight isomers of octamolybdates are known:a,b,c,d,e,f,gandh.Amongthemtheb-isomer isthemostcommon,whileisomerc,consideredaninter- mediate between a and b forms is also an important and frequently occurring ‘building block’ of many poly- molybdatestructures[52].CompoundA1isc-octamolyb- dateof4-methylpyridine.Theanionincludes14terminal oxygenatoms(Ooxo)(averageMo=Odistanceis
1.7104(49)A˚),6oxygensl2-O,4l3-Oand2l4-O.Whatis
more, in A1 complex a molybdenum-nitrogen bond occurs(Mo–N=2.249(2)A˚)whichischaracteristicforthisoctamolybdatetype.
Both A2 and A3 are b-type isomers, where A2 is octa- molybdate of 4-methylpyridine and A3 is octamolybdate of 4-methylaniline. The arrangement of b-octamolybdate anion is somewhat different than in the case of A1. TheMo atoms are surrounded only by O atoms. Eachanion
includes 14 terminal oxygen atoms (like in the c-octa-molybdate)averageMo=Odistanceis1.7007(88)A˚inthecaseofcompoundA2and1.6981(49)A˚forA3),6oxygens
l2-O, 4 l3-O and 2 l5-O. The b isomer is thermally more stable and more compact than c form. An b-octamolybdate anion is surrounded by organic cations and molecules of water, connected by a network ofhydrogen bonds. Crys- tallographic data for A3 is listed in the SI part.
formula. These rigid, zigzag chains built of distorted octahedra are linked by ionic interactions and hydrogen bonds with 3,5-dimethylanilinium cations. In this com- pound each MoO6octahedron contains two terminal oxy- gen atoms (Ooxo) and four l3-O oxygen atoms, that are linking 3 adjacent octahedra. Very similar structure was determined in the case of B4. Crystallographic data for B1, B2, B4 is listed in SI.
Four pentamolybdates C1–C4 belonging to a group of layered materials (2-dim) have been examined. As a starting point, we selected aniline and 4-methylaniline pentamolybdates C1, C2 [46,47]. To investigate the influence of substituent, we extended the group of inves- tigated compounds adding pentamolybdate of 4-bro- moaniline [48] and a new compound with a larger substituent, that is 4-ethylanilinum pentamolybdate (C4).
All discussed compounds have infinite anionic layers[(Mo5O16)2-]n,formedbydistortedMoO6octahedraandare surrounded by different cations: C1—anilinium, C2— 4-methylanilinium (p-toluidinium), C3—4-bromoanilinium and C4—4-ethylanilinium. In the structures of the layered pentamolybdates nearly flat, centro-symmetric blocks of 6 deformed MoO6 octahedra connected by their edges are present. Two boundary octahedra on both sides of each block are common to the two adjacent blocks, soeach formalunitconsistsof5MoO6individuals.Twooxygen
atomsatadistanceof*1.735A˚areboundtoeachofthe
molybdenum atoms. These O atoms are always incispositionrelativetoeachother.The(Mo5O16)2-anioncontains 10 oxygen atoms of this type, among them 6 are terminal atoms, wherein 4 are perpendicular to the plane of the layers. Each of the remaining four, strongly bonded oxygen atoms are common for two coordination polyhedra
ofneighbouringMonandMon’atoms(Mon-O*1.70A˚,
O-Mon,*2.42to2.74A˚).OctahedralcoordinationoffourMo atoms in each pentamolybdate unit is achieved through
anoxygenatomplacedatalongdistanceof*2.4to2.7A˚from Mo atom. We believe that the fragment: Mon-
Om…Mon’(whereMon-Om*1.74A˚,]Mon-Om…Mon,
*1658,Om-Mon,*2.60A˚)isacharacteristicfeatureofpentamolybdates.In(Mo5O16)2-unit6l2-Oand4l3-O
atoms are present (see Fig.1and SI for details for C4).
Three-dimensional hexagonal molybdenum trioxide D1 (3-dim) forms a system of parallel channels with adiameterof*5.8A˚,whichallowspenetrationofthechannelsby
monovalent ions (H?, Ag?, K?, Rb?, etc.) [49]. Forcomparisonpurposes,wehavealsotestedD2,acommer- ciallyavailableorthorhombicMoO3(POChGliwice).Itis
a layered compound with the distance between thick dou-blelayersofabout6.5A˚,whereasthedistancesbetween
atoms from adjacent layers, interacting through van derWaalsforces,areabout2.9to3.5A˚[50].
Group of one-dimensional (1-dim) polymeric
com-
pounds (with fibrous morphology) consists of compounds B1-B4. Since new compounds B1, B2 turned out to be chemically different, we tested additional compounds belonging to a family of polymeric molybdates. To verify the effect of the type and charge of cation, 1,3- phenylenediammonium trimolybdate B3 [45] was selected. To test the effect of organic cation we have undertaken efforts to synthesise trimolybdate of 4-methylaniline (B4). Both B3 and B4 have the same type of anion as B2 but different organic cation (cation charge is2?in the case of B3 and1?in B4).
In the case of B1 the infinite chain (without electric charge) is formed by Mo and O atoms, with a molecule of 1,2-phenylenediamine (pda) attached to every molybde- num atom. Formally, the compound may be treated as a hybrid molybdenum oxide with the composition of MoO3(pda). Each of the Mo atoms is coordinated by two nitrogen atoms of pda bringing the coordination number of Mo to 6. In each MoO4N2octahedron two terminal oxygen atoms, incisrelative position, are present, Mo=Ooxobond
lengthis1.7264(11)A˚.Twooppositeverticesineach
octahedron are occupied by l2-O atoms shared withadja- centoctahedra.
New 3,5-dimethylanilinium trimolybdate hydrate (B2) is
)2-
composed of infinite, anionic chains with (Mo3O
10 n
13

Molybdenum Complexes as Catalysts for the Oxidation of Cycloalkanes with Molecular Oxygen
1005
30
25
20
15
10
5
0
Fig. 1 Pentamolybdate building block and infinite layer, view along aaxis
Fig. 2 Oxidation of different cycloalkanes by Mo catalyst B2
Cyclooctanewasdeterminedtobethemostreactiveof all investigated cycloalkanes and the following order of catalyticreactivitywasestablished:cyclooctane[cyclo- hexane[cyclopentane. Consequently, cyclooctane was selectedforfurtherinvestigations.Allthecatalyticresults ofcyclooctaneoxidationwithmolecularoxygenaregath- eredinTable2andpresentedinFigs.2and3.Allapplied polyoxomolybdates were active as catalysts in theoxida- tion ofcyclooctane.
The A1-A3 compounds (0-dim) built of isolated octa- molybdate anions show moderate activity towards desired products. All compounds demonstrate quite similar selec- tivity towards ketone but A2 reaches only 50 % of selec- tivity towards alcohol in comparison with two other members of the series.
Compounds of the B series (1-dim) demonstrate high catalytic activity. Compound B1 shows the highest cat- alytic activity among all the studied catalysts. The
4 Catalytic Results
Three different cycloalkanes, viz. cyclopentane, cyclo- hexane or cyclooctane were applied as substrates (Scheme1) with molybdenum complex B2 as a represen- tativecatalyst.
The main products of cycloalkanes oxidation with molecular oxygen (from air) were cycloketone and cycloalcohol. No oxidation occurred at 393 K in the absence of the catalyst. For cyclopentane, only 2.9 % yield of ketone (TON=1090) and 0.8 % yield of alcohol (TON=300) was obtained in the presence of Mo catalyst B2 after 6 h (Fig.2). Under analogous conditions, cyclo- hexane was converted to ketone and alcohol with yields of 5.2 % (TON=1950) and 2.2 % (TON=830),respec-
tively. Finally, the oxidation of cyclooctane catalyzed by B2 resulted in 29.6 % yield for ketone (TON=11,100) and15.5%yieldforalcohol(TON=5812).
50
O
+
OH
40
cyclopentane
cyclopentanone
cyclopentanol
30
O
OH
Mocatalyst
+
O2
20
cyclohexane
cyclohexanone
cyclohexanol
10
O
OH
+
0
cyclooctane
cyclooctanone
cyclooctanol
B2
C2
Scheme 1 Oxidation of cycloalkanes
Fig. 3 Recycling and reuse of B2 and C2 molybdenum catalysts
13
Yield of ketone and alcohol, %
Yield of products, %
run I
run II
run III
run I
run II
run III

ketone alcohol

A.Szyman´skaetal.
1006
following order of catalytic activity was established: B1[B3[B2 C B4. B2 was twice recovered from the reactionmixtureandreusedinthecatalyticreaction.Yield of ketone and alcohol decreases insignificantly in the subsequent runs which is important for the possibility of recycling and reuse of molybdenum catalysts (Fig.3). HighercatalyticactivityofB3incomparisonwithB2and B4catalystsisintriguingtakingintoaccounttheidentical polymeric structure of the trimolybdateanion.
Layered compounds: C1–C4 (2-dim) demonstratediverse catalytic activity (Fig.4). C2 and C3 pentamolyb- dates show similar catalytic activity and selectivity towards the desired products. For C4 the selectivity to ketone slightly decreases while selectivity to alcohol increases significantly in comparison to C2 and C3 catalysts. C2 catalyst was recycled and reused with only a small change of catalytic activity (Fig.3) preserving the original crystal structure as indicated by XRPD studies.
It is important to state that for the whole series of C catalysts an additional product, suberic acid, wasidentified. Its formation is connected with the presence ofcycloalcoxy radical formed during the oxidation of cyclooctane (Scheme2) and stabilized between layers of C catalysts. The formation of suberic acid was found by XRPDanalysis of the solid phase left in the batch reactor after the oxi- dation reactionwith layered C1-C4 catalysts.
Considering the surface area values for compounds C1– C4, one can see that they are rather small, and it appears that surface is not the main factor determining catalytic activity (Table2). For example in case of C1 the biggest surface area was determined, whereas it is the worst cata- lyst in Cn family; exactly the opposite observation can be made in the case of C2. Similar observation can be made in case of compounds from B series.
Molybdenum oxides: hexagonal molybdenum oxide D1 and orthorhombic MoO3D2 show the lowest catalytic
narrow channels in three-dimensional covalent structure that may be too small for the reactants to enter into, seem tobethereasonbehindsuchpoorresults.
Summarizing, the best catalytic performance for oxida- tion of cyclooctane was observed for the polymeric B1, B3 and layered C2, C3 materials. The results obtained indicate that the catalytic activity is not only dependent on the structure of the inorganic anion, but also on other factors,
e.g. type of organic cation and its charge, crystal structure etc.
5 Discussion
Structural differences between the b and c-octamolybdate anions are relatively small (the same amount of oxo oxy- gens, andl2-Oatoms), which may explain quite similar catalytic activity. Slightly higher activity is observed for c- octamolybdate A1 in which 2 nitrogen atoms are directly connected to Mo atoms. Also, in the case of c-octa- molybdates average Mo=O distance is slightly longer than in the case of b-octamolybdates. The presence of nitrogen atoms directly connected to Mo atoms, which is also observed in one of the most active B1 catalyst, seems to be a factor contributing to a higher catalytic activity. However, the high activity of B3, C2, C3 (without Mo–N bonds) proves the existence of additional factors needed to betakenintoaccountwhendiscussingcatalyticactivity.
A very interesting observation is the high conversion of cyclooctane for hybrid polymeric molybdenum oxide B1.It seems that organic part of the compound improves liofility (wettability), whereas rigid inorganic-chain ensures the availability of catalytic centers (of yet unknown type) along the polymeric chain. In comparison, anionic poly- meric core in typical trimolybdates reduces the availability of catalytic centers along one-dimensional chain, by the presence of cations compensating its negative charge. This may be an explanation of the much lower activity of B2 and B4 in comparison to B1. These assumptions are con- firmed by high activity of the compound B3 (with exactly the same polymeric anion as in B2 and B4). In this case [NH3–C6H4–NH3]2?cations are present, and the number of these cations needed to neutralize the charge of anionic chain is halved with respect to B2 or B4. In this way the availability of the active centers increases byproviding‘‘free space’’along anionic chain unoccupied by the cations.
The high conversion of cyclooctane for C2 and C3 and its significantly higher value compared to C1 is surprisingdue to high similarity in chemical composition, structure of the anion and location and arrangement of the cations. Steric reasons may give a clue. For the reaction to proceed, cyclooctane molecules must be absorbed in the inter-layer
activity among the tested catalysts. Low availability
ofof
molybdenum-oxygen
catalytic
centres
and
a
system
50
40
30
20
10
0
C1
C2
C3
C4d(200)=15.18Å
d(200)=13.60Å d(200)=14.36Å d(200)=14.81Å
Fig.4OxidationofcyclooctanewithlayeredC1–C4compounds.In the lowest row interplanar d(200) spacings are given. Conversion indicates yield of ketone?alcohole
13
Yield [%]

ketone alcohole conversion ketone/alcohole*10 suberic acid

Molybdenum Complexes as Catalysts for the Oxidation of Cycloalkanes with Molecular Oxygen
1007
.
Scheme 2 Mechanism of cycloalkanes oxidation in the presence of polymolybdates catalysts

H
MoVIcomplex
+
+
H
(1)
OO.
.
+
(2)
O2
OO.
.
H
OOH

+

+
(3)
.

OO.

.
OO+
OH
O
(4)

+
+O2
.
OOH
MoVIcomplex
(5)
OO

+
H+
O.
+
.

OOHMoVcomplex
(6)
OH
O.

.
H
.
OH

.

+

+
(7)

.
layeredMoVIcomplex
O
O
H

H
(8)
O
OH
OH
O
O
OH+
+
MoVIcomplex
(9)
H O
1/2 O
H
2
2
space of pentamolybdates. Cyclooctane seems to require slightly more space than anilinium ion can provide, hence the low activity of the compound C1. Further, more detailed considerations included the examination of the impact of the distances between the layers on the catalytic activity. The yield of products for 4-methylanilinium
pentamolybdateC2[d(200)=14.36A˚]and4-bro-
moaniliniumpentamolybdateC3[d(200)=14.81A˚]issimilar. Figure4shows that there is an optimal distance
between layers [corresponding to the inter-planar spacing
d(200)] for the best catalytic performance. If the interlayerdistanceistoosmall,likeinC1[d(200)=13.6A˚],the
oxidation
reaction is more difficult to proceed
and the
formation of oxidation products (along with suberic acid)is suppressed. Increasing the distance between layers above the optimal size does not provide a clear benefit. It may even result in a decrease in catalytic activity, as is revealed for the C4 compound for which thedistance
d(200)=15.18A˚.Interplanard(200)spacingsusedin
Fig.4are derived from lattice constants and formulas of geometric crystallography. This value gives an estimation of space available between neighbouring layers in catalyst. Based on the yields of obtained products, correlation existing between d(200) and catalytic performance for very
13

A.Szyman´skaetal.
1008
similar compounds (C1–C4) seems to be reasonable and justified.
Pentamolybdate layers are open-framework construc- tions with variable thickness, which may allow for the oxygen to pass through the layers. Adsorbed molecule trapped in the oxidizing environment, may undergo further oxidation reactions leading to formation of suberic acid. For compounds A1–A3 (0-dim) or polymeric B1–B4 (1- dim), after the occurrence of a single process of oxidation, molecules of cyclooctanone or cyclooctanol can easily drift away from the catalyst surface through diffusion. In a qualitative manner, this also explains the lower ratio of ketone/alcohol for these catalysts (see Table2), and the lack of suberic acid in the reaction products.
Oxidation of alkanes was widely studied by many researchers. Oxidation of cyclohexane and cyclooctane with hydrogen peroxide as oxygen donor was performed in the presence of the CH3ReO3-PCA system. Formation of the cycloalkyl hydroperoxide, which was the main product in the cycloalkane oxidation, proceeded via free-radical mechanism[36].
Radical mechanism of cyclooctane oxidation was also observed for the reaction performed with H2O2at low temperature [41,42]. In contrast to our catalytic system, cyclooctyl hydroperoxide was the main reaction product.
Non-radical reaction mechanism of cycloalkane oxida- tion was described by [53] using t-butyl hydroperoxide and peracetic acid as oxygen donors and ruthenium catalyst. The reaction proceeds through the oxo-ruthenium species. In this case the reaction was carried out in the presence of radical sacavenger .
Similar catalytic systems based on polyoxometalates as catalysts were studied in the cyclooctane oxidation with molecular oxygen [54]. Introduction of cobalt ion into heteropoly structure significantly influences the catalytic activity and selectivity in the studied reaction. The amount of cyclooctyl hydroperoxide formed during the reaction was negligible.
Salen metallocomplexes were also investigated in the same reaction conditions [55]. Catalytic activities of salen complexes and polymolybdates are similar, selectivity to cycloketone is different, though.
Based on the literature [56–61] and our investigations, we suggest the following oxidation mechanism in the presence of polymolybdate catalysts (Scheme2).
According to Sheldon and Kochi [56] the oxidation of cycloalkanes with molecular oxygen proceeds via free- radical mechanism. The radical chain reaction mechanism of this reaction was experimentally confirmed by us, showing almost complete inhibition of cyclooctane oxida- tion in the presence of a free radical scavenger 2,6-di-tert- butyl-p-cresol (DBPC).
A hypothetical set of reactions is presented in Scheme2. Except cycloketone and cycloalcohol, which are the major products of this reaction, small amounts of cyclohy- droperoxide are observed but the formation of ring-opened side-products like di-carboxylic acids is also possible through this mechanism. It is well-known that the selective catalytic oxidation of C-H bonds results in the formation of hydroperoxides [36–38]. For the investigated polymolyb-datesonlytracesofhydroperoxide(\0.1%)weredetectedafter 6 h of reaction which is indicative of polymolybdates as good catalysts for hydroperoxides decomposition.
The first step of the whole process is a slow reaction of the cycloalkane with polymolybdate resulting in the abstraction of hydrogen from hydrocarbon to form cycloalkyl radical R•(Reaction 1), which acts as the ini- tiation of chain reaction [57–59]. The newly formed spe- cies can react further with molecular oxygen in the chain- propagation step to the cycloperoxyl radical ROO•(Reac- tion 2). This in turn reacting with cycloalkane gives
R•
cyclohydroperoxide ROOH and cycloalkyl radical
(Reaction 3). Recombination of cycloperoxyl radicals ROO•is a first source of cycloketone and cycloalcohol constituting the major chain-termination step (Reaction 4). Cyclohydroperoxide can be decomposed in a heterolytic [56,60] or homolytic [56,61] manner. The heterolytic decomposition of cyclohydroperoxide catalyzed by molybdenum catalyst produces cycloperoxyl radical
ROO•(Reaction 5) while cycloalkoxyl radical RO•and hydroxyl radical OH•are produced in homolytic decom- position (Reaction 6). Majority of cycloalcohol is produced
in Reaction 4. Additional amount of cycloalcohol origi- nates from abstraction of hydrogen from cycloalkane by cycloalkoxyl radical (Reaction 7). Cycloalkoxyl radicals can also undergo a b-cleavage of C–C bond [62–65] yielding the ring-opened x-formyl radical CHO–(CH2)6– CH2 which is the precursor for obtaining di-carboxylic acid (Reaction 8). However, the literature dealing with cycloalkane oxidation claims that cycloketone is the most important precursor of ring–opened by-products [56–61]. In all our catalytic tests the yield of cycloketone is higher than the yield of cycloalcohol. This is a clear indication that cycloketone can be formed not only in Reaction 4 but alsointheoxidationofthecycloalcohol(Reaction9).
To sum up the discussion, we have to consider all the data which characterize the investigated compounds (also data gathered in SI). In particular:
–
Formation of CO and CO is not observed during the
2
oxidation of cycloalkanes.
–
Stability of compounds in reaction conditions was indicated by XRPD studies versus temperature (see Supporting Information).
13

Molybdenum Complexes as Catalysts for the Oxidation of Cycloalkanes with Molecular Oxygen
1009
–
Recoverability and reusability of catalysts (B2, C2) with only a small change of catalytic activity of fresh and spent samples were confirmed (Fig.3).
Compounds B1 and C2 boiled in cyclooctane (Tbhigher than the temperature of reaction) remain unchanged (see Supporting Information). Furthermore, compounds of C series were synthesized from the reaction mixture containing boiling water solution (pH 2). Since the catalysts were synthesized in rather severe conditions, their solubility in cycloalkane in given reaction conditions isdoubtful.
Rather obvious dependence of catalytic activity on cationic charge in compounds B2–B4 was observed.Dependence of catalytic properties on interplanar d(200) spacing in the case of C1–C4 was demonstrated. Low surface area for all the investigated compounds
The most active compounds B1, B3, C2, C3 are stable up to about 200°C (temperature dependent XRPD, see Supporting Information). What is more, catalysts are recoverable and reusable, which indicates the possibility of practicalapplications.
The catalytic properties of these materials are complex features resulting from their crystal structure and chemical composition. The interesting catalytic activity can be observed for one-dimensional (polymeric) or two dimen- sional (layered) materials. For the layered materials the highest catalytic activity is obtained after adjusting proper, optimal distance between layers. For the anionic polymers B2, B4 higher blocking of molybdenum catalytic centers (by cations) decreases the activity of the catalyst.
–
–
–
Acknowledgments The research has been partly supported by the EU Human Capital Operation Program, Polish Project No. POKL.04.0101-00-434/08-00. The research was carried out with the equipment purchased thanks to the financial support of the European Regional Development Fund in the framework of the Polish Inno- vation Economy Operational Program (contract no. POIG.02.01.00- 12-023/08). The authors also wish to acknowledge the synchrotron centres: DIAMOND and DESY for diffraction measurements. CCDC—1041613,909664,1042866,1042865,1041614containthe
supplementary crystallographic data for compounds A3, B1, B2, B4, C4, respectively. These data can be obtained free of charge from The Cambridge Crystallographic Data Centre viawww.ccdc.cam.ac.uk/data_request/cif.
–
and no obvious correlation catalytic activity indicate the other than the surface area.
between surface and significance of factors
All these observations allow us to draw a final conclu- sion that the crystal structures of the catalysts investigated by us are important factors in the catalytic process. This also supports the heterogeneous character of the catalytic reaction, at least in the case of the most stable B1, B3, C1– C4 catalysts.
Open Access This article is distributed under the terms of the Creative Commons Attribution 4.0 International License (http://creativecommons.org/licenses/by/4.0/), which permits unrestricted use, distribution, and reproduction in any medium, provided you give appropriate credit to the original author(s) and the source, provide a link to the Creative Commons license, and indicate if changes were made.
6 Conclusions
The first example of oxidation reaction ofcycloalkanes with molecular oxygen without solvent and co-reductor that involves polymolybdate complexes as catalysts isreported.
Polymolybdates with anions in the form of isolatedclusters A (0-dim), compounds with polymeric anions B (1-dim), layered materials C (2-dim) as well as hexagonal and orthorhombic molybdenum oxides D (3- dim) were selected, synthesized and physico-chemically characterized (if needed) and applied in the process ofcatalytic oxidation of cycloalkanes. Among them A3,B1, B2, B4, C4 polymolybdates were synthesized for the firsttime.
All the synthesized compounds were active in theinvestigated reaction. For series of B and C catalysts high catalytic activity was observed. Moreover, for the series oflayered C catalysts the oxidation of cyclooctane to cyclooctanone and cyclooctanol is accompanied by theformation of suberic acid (COOH)–C6H12–(COOH). For-mation of suberic acid is observed for layered poly- molybdates only. Product yields for C series seem to be
References
1. Enemark JH, Cooney JJA, Wang J-J, Holm RH (2004) ChemRev 104:1175–1200
2. Lyashenko G, Saischek G, Judmaier ME, Volpe M, BaumgartnerJ,BelajF,JancikV,Herbst-IrmerR,Mo¨sch-ZanettiNC(2009)Dalton Trans29:5655–5665
3. Yin GC (2010) Coord Chem Rev 254:1826–1842
1. HilleR,HallJ,BasuP(2014)ChemRev114:3963–4038
2. Cindric´M, Novak TK,Krajlevic´S, Krajl M, Kamenar B (2006) Inorg Chim Acta359:1673–1680
3. CartuyvelsE,VanHeckeK,VanMeerveltL,Go¨rller-WalrandC,Parac-VogtTN(2008)JInorgBiochem102:1589–1598
4. Cindric´M, Veksli Z, Kamenar B (2009) Croat Chem Acta 82(2):345–362
5. Djordjevic C, Puryear BC, Vuletic N, Abelt CJ, Sheffield SJ (1988) Inorg Chem27:2926–2932
6. DickmanMH,PopeMT(1994)ChemRev94:569–584
7. ThielWR(1997)JMolCatalA:Chem117:449–454
8. JiaM,ThielWR(2002)ChemCommun20:2392–2393
9. Pereira CCL, Balula SS, AlmeidaPaz FA, Valente AA, Pillinger M, Klinowski J, Goncalves IS (2007) Inorg Chem46:8508–8510
]2-
affected by inter-layer distance between [Mo O
5 16 n
anions.
13

A.Szyman´skaetal.
1010
1. Szyman´skaA,NitekW,MuchaD,KarczR,PaminK,PołtowiczJ, Łasocha W (2013) Polyhedron60:39–46
2. MairRD,GraupnerAJ(1964)AnalChem36:194–204
3. ShulpinGB, Kozlov YN, Shulpina LS, Kudinov AR, Mandelli D (2009) Inorg Chem48:10480–10482
4. ShulpinGB, Kozlov YN, Shulpina LS, Petrovskiy PV (2010) Appl Organometal Chem24:464–472
5. Szyman´skaA,NitekW,Rutkowska-Z_bikD,ŁasochaW(2014)Monatsh Chem145:921–929
6. Roma´nP,Gutie´rrez-ZorrillaJM,Mart´ınez-RipollM,Garc´ıa-Blanco S, Cryst J (1987) Spectrosc.17:109–119
7. ŁasochaW, Rafalska-Łasocha A, Grzywa M, Gaweł B (2008)Catal Today137:504–509
8. ŁasochaW,SchenkH(1997)JApplCryst30:909–914
9. OszajcaM, Smrcok L, Łasocha W (2013) Acta Cryst 69:1367–1372
10. ŁasochaW, Grzywa M, Oszajca M, Kristallogr Z (2009) Suppl 30:387–394
11. GuoJ, Zavalij P, Whittingham M (1994) Eur. J. Sol. State Inor.31:833
12. GruberH,KrautzE(1980)PhysStatusSolidiA62:615
13. Brandenburg K, Putz H, Diamond: crystal and molecular struc-ture visualization crystal impact. GbR, Postfach 1251. D-53003 Bonn
14. AllisDG, Rarig RS, Burkholder E, Zubieta J (2004) J Mol Struct 688:11–31
15. MurahashiSh-I, Komiya N, Oda Y, Kuwabara T, Naota T (2000) J Org Chem65:9186–9193
16. PaminK,JachimskaB,OnikK,PołtowiczJ,GrabowskiR(2009) Catal Lett127:167–174
17. PołtowiczJ, Pamin K, Tabor E, Haber J, Adamski A, Sojka Z (2006) Appl Catal A299:235–242
18. SheldonRA, Kochi JK (1981) Metal catalyzed oxidations of organic compounds. Academic Press,London, pp 34–70
19. Hermans I, Jacobs PA, Peeters J (2006) J Mol Catal A: Chem 251:221–228
20. MishraGS, Frausto de Silva JJR, Pombeiro AJL (2007) J MolCatal A Chem265:59–69
21. HermansI,PeetersJ,JacobsPA(2008)TopCatal48:41–48
22. TraylorTG(1987)FengXu.JAmChemSoc109:6201–6202
23. MansuyD, Bartoli J-F, Momenteau M (1982) Tetrahedron Lett 23:2781–2784
24. BarclayLRC, Lusztyk J, Ingold KU (1984) J Am Chem Soc 106:1793–1796
25. DrulinerJD, Krusic PJ, Lehr GF, Tolman CA (1985) J Org Chem50:5838–5845
26. BeckwithALJ,HayBP(1989)JAmChemSoc111:230–234
27. OlivellaS,SoleA(1991)JAmChemSoc113:87–94
1. Brito JA, Teruel H, Muller G, Massou S, Gomez M (2008) Inorg Chim Acta361:2740–2746
2. Abrantes M, Amarante TR, Antunes MM, Gago S, Paz FAA, Margiolaki I, Rod-rigues AE, Pillinger M, Valente AA, Gonca- lves IS (2010) Inorg Chem49:6865–6873
3. Pisk J, Agustin D, Vrdoljak V, Poli R (2011) Adv Synth Catal 353:2910–2914
4. Pisk J, Prugovecki B, Matkovic-Calogovic D, Poli R, Agustin D, Vrdoljak V (2012) Polyhedron33:441–449
5. Amarante TR, Neves P, AlmeidaPaz FA, Pillinger M (2012) AA Valente. I Inorg Chem Comm20:147–152
18. Rayati S, Rafiee N, Wojtczak A (2012) 386:27–35
Inorg Chim Acta
1. Masteri-Frhani M, Kashef Z (2012) J Magn Magn Mater 324:1431–1434
2. GrivaniG,AkheratiA(2013)InorgChemComm18:90–93
3. Djordjevic C, Puryear BC, Vuletic N, Abelt CJ, Sheffield SJ (1997) Inorg Chem36:1798–1805
1. Das S, Bhowmick T, Punni-Yamurthy T, Dey D, Nath Chaudhuri MK (2003) Tetrahedron Lett44:4915–4917
2. Gharah N, Chakraborty S, Mukherjee AK, Bhattacharyya (2004) Chem. Comm.22:2630–2632
J,
R
1. Bregeault J-M, Vennant M, Salles L, Piquemal J-Y, Mahha Y, Briot E, Baka-la PC, Atlamsani A, Thouvenot R (2006) J Mol Catal A Chem250:177–189
2. Mancka M, Plass W (2007) Inorg Chem Commun10:677–680
3. Gharah N, Chakraborty S, Mukherjee AK, Bhattacharyya R (2009) Inorg Chim Acta362:1089–1100
4. Madeira F, Barroso S, Namorado S, Reis PM, Royo B, Martinsm AM (2012) Inorg. Chim Acta83:152–156
5. Bagherzadeh M, Amini M, Parastar H, Jalali-Heravi M, Ellern AA,KeithWooL(2012)InorgChemCommun20:86–89
6. Carrasco CJ, Montilla F, Alvarez E, Herbert M, Galindo A(2013) Polyhedron54:123–130
7. Sensato FR, Custodio R, Longo E, Safont VS, Andres J (2003) J Org Chem68:5870–5874
8. Pontes da Costa A, Reis PM, Gamelas C, Romao CC, Royo B (2008) Inorg Chim Acta361:1915–1921
9. Bagherzadeh M, Tahsini L, Latifi R, Ellern A, KeithWoo L (2008) Inorg Chim Acta361:2019–2024
10. Bagherzadeh M, Mehdi Haghdoost M, Amini M, Derakhshandeh PG (2012) Catal Commun23:14–19
11. Bagherzadeh M, Amini M, Ellern A, KeithWoo L (2012) Inorg Chem Commun15:52–55
1. Herrmann WA, Lobmaier GM, Priermeier T, Mattner ScharbertB(1997)JMolCatalAChem117:455–469
2. ShulpinGB(2002)JMolCatalAChem189:39–66
MR,
1. PołtowiczJ,HaberJ(2006)JMolCatalAChem250:177–189
2. Duprez D, Cavani F (2014) Handbook of advanced methods and processes in oxidation catalysis. Imperial College Press, London, pp320–333
13