Availableonlineatwww.sciencedirect.com

ScienceDirect

EnergyProcedia97(2016)23–30

EuropeanGeosciencesUnionGeneralAssembly2016,EGUDivisionEnergy,Resources&Environment,ERE

## MetalsAccumulationDuringThermalProcessingofSewageSludge
-CharacterizationofFlyAshandAirPollutionControl(APC)Residues

MonikaKasinaa,*,PiotrR.Kowalskia,MarekMichalika

aInstituteofGeologicalSciences,JagiellonianUniversity,Oleandry2a,30-063Krakow,Poland

Abstract

SewagesludgethermalutilizationleadstoproductionofflyashandAPCresidueswhichmaycontainelevatedamountsofsomemetallicortoxicelements(Fe,Zn,Pb,Sn,Au,Hg,Cd,As).DistributionoftheseelementsinstudiedflyashandAPCresidueswasunequalanddependentontheirmeltingtemperature.MetalsinflyasharepresentasFe-richgrainsandrimsaroundSi-glasswhereasinAPCmetalliccomponentsaremostlyrepresentedbySn-richinclusionsdispersedinmatrix,Ca-phosphatesorasseparatemicro-grains.Elementsconcentrationswereelevatedbutoverallcontentwaslowthusdisqualifyingthematerialintermsofrecovery.
©2016TheAuthors.PublishedbyElsevierLtd.
Peer-reviewunderresponsibilityoftheorganizingcommitteeoftheGeneralAssemblyoftheEuropeanGeosciencesUnion(EGU).

©2016TheAuthors.PublishedbyElsevierLtd.ThisisanopenaccessarticleundertheCCBY-NC-NDlicense(http://creativecommons.org/licenses/by-nc-nd/4.0/).
Peer-reviewunderresponsibilityoftheorganizingcommitteeoftheGeneralAssemblyoftheEuropeanGeosciencesUnion(EGU)

Keywords:thermalutilization;sewagesludge;flyash,airpollutioncontrolresidues;metalliccomponents

### Introduction

Duetoincreasingmassofsewagesludgeproducedinwastewatertreatment,problemsinitsmanagementhaveappearedinPoland.Overyearssewagesludgewaslandfilled,howeverduetotheEuropeanLandfillDirective1999/31/EC[1]itisnotanoptionanymoreduetothefactthatsewagesludgecontainsmaterialsregardedashazardous.

*Correspondingauthor.Tel.:+48-607-443-607;fax:+48-12-633-22-70.
E-mailaddress:monika.kasina@uj.edu.pl

1876-6102©2016TheAuthors.PublishedbyElsevierLtd.ThisisanopenaccessarticleundertheCCBY-NC-NDlicense(http://creativecommons.org/licenses/by-nc-nd/4.0/).
Peer-reviewunderresponsibilityoftheorganizingcommitteeoftheGeneralAssemblyoftheEuropeanGeosciencesUnion(EGU)doi:10.1016/j.egypro.2016.10.012

Highlyconcentratedmetallicandharmfulelements,toxicorganicsubstancesandbiologicalcomponents(e.g.parasites,microbes)disqualifythismaterialforlandfilling.InadditionEU-memberstatesobligedthemselveswithaccordancetothatdirectivetoreducetheamountofbiodegradableswastelandfillby65%incomparisontotheamountfrom1995[2].SomeoftheEUcountries(Germany,TheNetherlands,Sweden,Austria,DenmarkandBelgium)achievedthegoalalreadyin2010bycombiningmaterialrecycling,biologicaltreatmentandwaste-to-energytechnology[2],howeverinPolandstillover50%ofwasteislandfill[3].
CurrentlyinEuropeoneofthemostreasonablemethodforsewagesludgetreatmentisincineration[4,5].Thisprocessresultsintheutilizationofsewagesludgebythermaldestructionoftoxiccompounds[6]withminimumenergyconsumptionandthusminimizethecostsofmanagingwastegeneratedintheprocess.Inadditionenergyisrecoveredduetohighcalorificvalueofsewagesludge,almostequaltothatofbrowncoal[5].Neverthelesseventheincinerationhasadvantagesduetothereductionofsewagesludgevolumeandlowerdisposalcostsitisnotacompletemethod[7]sincealmost30%ofthesolidsremaininincinerationresiduesasflyashandairpollutioncontrol(APC)residues.
ThegoalofthisstudywastocharacterizechemicalandmineralcompositionofflyashandAPCresiduesaswellastoattempttocharacterizefractionationofmetallicandtoxicelementsandtheiraccumulationwithinresiduematerialsintermsoftheirpotentialrecovery.

### Materials&methods

  1. Characteristicofsewagesludgethermalutilizationplant–technologicalapproach

Dewateredsludgeistransporteddirectlyfromwastewatertreatmentplantbyconveyorstothedewateredsludgesilo,whereitisfurthertransportedtothenodeforsludgemembranedryingsystemdownto22%drymass.Thedryerissuppliedwithheatintheformofhotsteam,whichisrecoveredfromtheincinerationprocess.DriedsludgeisincineratedinthefluidizedbedfurnacePyrofluid™whichischaracterizedbyhighturbulenceofthefluidizedbedataconstanttemperatureandconstantintensityoftheprocesswhichprovidescompleteincinerationoforganicmatter,constantoperatingtemperatureintherangeof850-900ºCwhatensuresalongerlifetimeofthefurnaceandtheeffectivereductionofNOxemission.Inadditiontheheatexchangeareawithinthefluidbedallowstoreducethesizeoftheinstallation.Athermalutilizationstationisequippedwithaheatexchanger,responsibleforpre-cooloffluegasesandtheproductionofsaturatedsteamtopowerthedryingnode[8].

  1. Materialscharacteristicandpreparationforanalyses

Duringtheprocessofsewagesludgethermalutilizationaflyash,classifiedasnon-hazardouswaste1andby-productsfromthecleaningofexhaustgasessocalledairpollutioncontrolresidues(APC)residues,classifiedashazardouswaste2wereproduced.
Flyashwasareddish,fine-grainedmaterial,containing~30wt%ofparticleswithin0.25-0.063mmsizerangeandverylowsolublematerialcontent(~1wt%),whereasAPCresidueswerelightgrey,veryfine-grainedmaterial,whereparticlesbetween0.25-0.063mmsizeconstituteover~99wt%andthesolublematerialcontentwasca.98wt%.
DuetohighcontentofsolublematerialinAPCresiduesasolublefractionwasremovedbydissolutionindeionizedwater(APCc),whatcausedsignificantmassreductionof98%andadditionalconcentrationofpotentiallyvaluableortoxicmetals.

1. Flyash(wastecode:190114)withaccordancetotheRegulationoftheMinisteroftheEnvironmentof9December2014(Dz.U.2014poz.1923)isdefinedas:“ashotherthanthosementionedin190113(flyashcontainingdangeroussubstances)”.

2. APCresidues(wastecode:190107*)withaccordancetotheRegulationoftheMinisteroftheEnvironmentof9December2014(Dz.U.2014
poz.1923)isdefinedas:“solidwastefromgastreatment”.

  1. Analyticalmethods

Thechemicalcompositionofsewagesludgeincinerationresidueswasanalyzedusinginductivelycoupledplasmamassspectrometry(ICP-MS)andinductivelycoupledplasmaopticalemissionspectrometry(ICP-OES)methodsperformedintheACMEAnalyticalLaboratoriesLtd,Vancouver,Canada.ThemainmineralcompositionwasdeterminedusingaPhilipsX’PertDiffractometer(APDtype)withaPW3020verticalgoniometer.TheanalyticalrangeforXRDanalyseswas2-64°e,CuKaradiation,astepsizeof0.02°andatimeof1s/stepwereapplied.Forphaseidentification,thePhilipsX’PertGraphicsandIdentifyv.1.2asoftwarewiththeICDDPDF2databasewasused.Tocharacterizetheformofoccurrencesofmetalliccomponentsandtheircompositionafieldemissionscanningelectronmicroscope(FE-SEM)HitachiS-4700wasused.Quantitativeanalysesofthechemicalcompositionofthemetallicparticleswasperformedusinganenergydispersivespectrometer(EDS).Theflyash,andAPCresidues,preparedasthinsections,werecarboncoatedandexaminedwithFE-SEMoperatingatanacceleratingvoltageof20kV,usingthebackscatteredelectrons(BSE)mode.

### Resultsanddiscussion

  1. MineralandchemicalcompositionofflyashandAPCresidues

TheflyashwasaSiO2-P2O5-Fe2O3-CaOdominatedmaterial(35wt%SiO2,17.92wt%P2O5,15.85wt%Fe2O3and12.63wt%CaO).TheXRDanalysesindicatedthepresenceofquartz(SiO2),apatite(Ca5(PO4)3(OH,F,Cl)),hematite(Fe2O3)andfeldspar(K(AlSi3O8)-Na(AlSi3O8)-Ca(Al2Si2O8))asmainmineralphases.Howeverintheliteraturewhitlockite(Ca3(PO4)2)ismentionedmoreoftenthanapatite[9].Thecontentofmetallicandtoxicelementsinflyashwashigh.ContentsoftheseelementsarecomparedinTable1totheuppercontinentalcrust[10].

Table1.Contentofselectedmetallicandtoxiccomponentsinflyash,APCresiduesandAPCc(inbold–highlyconcentratedelementsinstudiedmaterials).

Element	Unit	Flyash	APC

APCc	Uppercontinental
residues	crustcomposite[10]

Fe	%	11.09	0.06	1.42	5.544
Ti	%	0.59	0.01	0.09	0.64
Mn	%	0.09	0.001	0.02	0.1
Mo	ppm	25.5	1.1	4.5	1.1
Ni	ppm	119.5	1.6	43.3	47
Cr	ppm	1047	0.001	89	92
Zn	ppm	4472	164	6326	67
Cu	ppm	665.5	12.2	476.6	28
Pb	ppm	138.0	14.8	514.3	17
Sn	ppm	364	66	2465	2.1
Co	ppm	27.2	0.3	8.6	17.3
As	ppm	16.2	0.4	15.4	4.8
Cd	ppm	7.0	0.5	20.3	0.09
Sb	ppm	6.9	2.1	64.6	0.4
Hg	ppm	0.01	10.05	50.00	0.05
Au	ppm	0.9	0.00018	0.00005	0.00015

TheAPCresiduescompositionwasdominatedbysolubleminerals,mostlythenardite(Na2(SO4)).Thenarditecouldforminthereactionofsodiumbicarbonate(NaHCO3)whichwasusedasareagentduringthepurificationoffluegases(i.a.removalofSOx).Asignificantmassreductionof98wt%relatedtotheremovalofsolublematerialbydissolutionindeionizedwatercaused30-foldadditionalconcentrationofsomeelements.MainmineralphasesdetectedinAPCresiduesafterremovalofsolublematerials(APCc)werequartz,calcite(Ca(CO3))andapatite.InTable1arelistedthemetallicandtoxiccomponentspresentinAPCresiduesandhighlyconcentratedinAPCc.
TheconcentrationofREEandothercriticalelementswasverylow,andincomparisontotheuppercontinentalcrustsignificantlydepleted.However[11]indicatedincrust-normalizedREEpatternofsewagesludgeashproducedinJapanisslightlyenrichedwithSm,Eu,andTb.Neverthelesswemustkeepinmindthatsewagesludgeincinerationresiduescandifferincompositionandcontentofvariouselementsdependingonthelocalenvironmentalconditions,levelofenvironmentalawareness,economicdevelopment,andalsosocialneedsandsocietyeducationineachregion.

  1. ElementsfractionationbetweenflyashandAPCresidues

Thepartitioningbehaviorofelementswaswidelystudiedforcoalcombustion.Threemainclassesaredistinguishedbasedontheelementvolatility[12,13]:non-volatile,partiallyvolatileandhighlyvolatile.

Fig.1.Metalfractionationofsewagesludgeincinerationresidues.	-relativeenrichmentofelementsinAPCc;	-relativeenrichmentofelementsinflyash;XAPCc/XflyashforAswas~1;boilingtemperaturesofelementsfrom[14].

Someelementscanoverlapbetweenthesethreegroupsdependingone.g.combustionconditionsandcombustortypewhatcancausedifferentrangesofvolatilityoftheelementsaswellasfluiddynamicsandkineticfactorswithintheincinerator[15].
Eventhoughtherangeofvolatilityoftheelementscanbelargeassuggestedby[13]atsomepointitwaspossibletonoticesimilaritiesinelementsvolatilityseriesinsewagesludgethermalincinerationresiduesandcoalcombustionresidues.
ThedistributionofmetalsinflyashandAPCresiduesafterincinerationinthefluidizedbedfurnacewasanalyzedbycomparingmetalconcentrationsintheflyashandAPCc.AmetalenrichmentfactorwascalculatedfromtheratioofconcentrationofgivenelementinAPCctoconcentrationinflyash(XAPCc/Xflyash).Thevaluesbelow1indicatedtheconcentrationofelementsinflyashwhereasthevaluesabove1indicatedtheenrichmentofelementsintheAPCresidues(Figs.1,2).
TheboilingandmeltingtemperaturewereexaminedtoshowthecorrelationofXAPCc/XflyashwithtemperatureinordertodemonstratewhichofthesefactorswasresponsibleformetaldistributionbetweenflyashandAPCresidues.

Fig.2.Metalfractionationofsewagesludgeincinerationresidues.	-relativeenrichmentofelementsinAPCc;	-relativeenrichmentofelementsinflyash;	-almostequallydistributedelements;XAPCc/XflyashforAswas~1;meltingtemperaturesofelementsfrom[14].

BoilingtemperaturepoorlycorrelatedwiththeXAPCc/Xflyashcouldbeappliedonlytosomeelements(Fig.1).Accordingto[13],volatilityofelementsusuallyshowsapositivecorrelationwiththeirboilingpoints.Howeverinthatstudyenrichmentofflyashincomparisontobottomashwasshown.Forsewagesludgeincinerationresiduesdiscrepancieswereobserved,mostlyduetothefactthatbottomashwasnotproducedatallandthefractionofthefly

ashandAPCresidueswasmuchfiner.AssuggestedbyWilczyńska-Michaliketal.andMardonandHower[16,17]elementsconcentratemoreeasilyonafinerparticlesduetolargersurfaceareaofafractionandcanbedependentonbothmeltingorboilingtemperature.NeverthelessotherfactorsresponsibleformetalfractionationbetweenflyashandAPCresiduesshallalsobeconsideredinthefurtherstudies.
MeltingtemperatureofelementscorrelatedwiththeXAPCc/XflyashratioandseemedtobethemainfactorgoverningtheirpartitioninginflyashandAPCresidues(Fig.2).Elementscharacterizedbyhighmeltingtemperaturewere
mostlyconcentratedinflyash(e.g.Mo,Cr,Ti,Fe,Ni,Co,Mn,Cu,Au),theseofalowermeltingtemperaturecouldbeledoutfromthefurnaceinthevolatileformandconcentratedinAPCresidues.OnlyAs,ZnandCuweredistributedequallybetweenflyashandAPCresidues.ThesefindingswereinagreementwithElledetal.[18]whoalsosuggestedHg,Cd,Sb,AsandPbtobevolatilizedduringtheincinerationandtheircondensationonashsurfaceduringthetemperaturedropdownrelatedtothefluegasesheatrecovery[19].

Fig.3.(a)grainofFeox;(b)rimsaroundsilicaglasscomposedofFeox;(c)Ni-Fe-Cralloys;(d)roundedphosphatewithSn-Tirichinclusions;(e)roundedphosphatewithSn-Tirichinterstitions;(f)grainscontainingSi,Pb,K(Pb-Ksilicide);
(f)grainscontainingSi,Fe,Ni(Fe-Nisilicide);(g)Ti-Fealloy;(h)multi-metallicgrainrichinBa,Ti,ZnandFe.

  1. TheformsofoccurrenceofmetalliccomponentsinflyashandAPCresidues

Ironoxides(Feox)intheformofseparategrainsupto20μminsize(Fig.3a)orintheformofrimsaroundgrainsofsilicaglassorothermatrixcomponentsofflyash(Fig.3b)werethemostcommonmetaloccurrencesinflyash.FeoxwereoftendispersedwithinCa-phosphates.SinglegrainsofFe-phosphateswerealsodetected.Othersingle

grainscontainingmetalswererichinCr,FeandNiwhichincompositionwerethenearesttoNi-Fe-Cralloys(Fig.3c).
InAPCresiduesmetalliccomponentsweredispersedchaoticallyinthematrixintheformofinclusions.Roundedphosphategrainsuptodozensofμmindiameterwhichcontaininclusions(Fig.3d)orinterstitions(Fig.3e)composedofSnwithadmixturesofTiwerecommon.Metalliccomponentswerealsopresentintheformofseparatedelongatedgrainsupto50μminsizewhichwerecomposedofSi,PbandK(Fig.3f)orSi,FeandNi(Fig.3g).GrainswerepreliminaryidentifiedassilicidesofPbandKorFeandNi.Theexistenceofsilica-richphasescanbeexplainedbythefactthat,influidizedbedincinerators,thecombustionbedmaterialusuallyconsistsofsilicasand,neverthelesssewagesludgeitselfcancontainhighconcentrationofsilicawhichoriginatefromthecitysewagesystemintowhichwatertogetherwiththestreetsandcanflowin.AlsosingleexamplesofTi-Fealloysuptoμminsize(Fig.3h),aswellasmulti-elementgrainsrichinBa,Ti,Zn,FeandSn,cubic,withasizeupto40μm(Fig.3i)werefound.

### Conclusions

Themetallicelementsaccumulatedinthesewagesludgeincinerationresidueswerepresenteitherintheformofseparategrainsormulti-elementmixturesaswellasrimmingSi-richcomponents,howevertheoverallcontentofthemwasnothigh.AlthoughtheincinerationresidueswereenrichedincomparisontotheaveragecompositionofuppercontinentalcrustinmetalsandtoxicelementssuchasCu,Zn,Pb,Ni,As,Cd,Au,Hg,Sn,Cr,Sb,Co,theoverallconcentrationofmetalswasverylow.Inflyashthetotalconcentrationwasnothigherthan12wt%,whereof11wt%wasFe.InAPCcthetotalcontentofmetalshardlyexceeded2wt%.ThepartitioningofmetalsbetweenflyashandAPCresidueswasrelatedtothemeltingtemperatureofelementsandconditionswithintheincinerationchamber.
Duetolowcontentofvaluablemetalstheirrecoveryisnotaneconomicallyjustifiedoptions.Howeverduetoaquitehighphosphatecontentandlowcontentofpotentiallyhazardouselementstheflyashcanbeconsideredassuitablematerialforfertilizer.IncaseofAPCresiduesfurtherprocessingisrequiredtoadaptmaterialforfurtherusageduetohighcontentofundesirableselementse.g.Hg,As,Cr.

### Acknowledgements

ThestudywassupportedbyPolishNationalScienceCentre(NCN)grantnumberUMO-2014/15/B/ST10/04171.

### References

[1]CouncilDirective199/31/ECof26April1999onthelandfillofwaste.OfficialJournaloftheEuropeanCommunities1999;L182,1-19.
[2]CaneghemVanJ,BremsA,LievensP,BlockC,BillenP,VermeulenI,DewilR,BaeyensJ,VandecasteeleC.Fluidizedbedwasteincinerators:Design,operationalandenvironmentalissues.ProgEnergyCombustSci2012;38(4),551-582.doi:10.1016/j.pecs.2012.03.001.
[3]http://ec.europa.eu/eurostat/statistics-explained/index.php/Waste_statistics.
[4]StastaP,BoranJ,BebarL,StehlikP,OralJ.Thermalprocessingofsewagesludge.ApplThermEng2006;26(13):1420-1426.doi:10.1016/j.applthermaleng.2005.05.030.
[5]FytiliD,ZabaniotouA.UtilizationofsewagesludgeinEUapplicationofoldandnewmethods-Areview.RenewSustEnergRev2008;12:116-140.doi:10.1016/j.rser.2006.05.014.
[6]KhiariB,MariasF,ZagroubaF,VaxelaireJ.Analyticalstudyofthepyrolysisprocessinawastewatertreatmentpilotstation.Desalination2004;167:39-47.doi:10.1016/j.desal.2004.06.111.
[7]MaleriusO,WertherJ.Modellingtheadsorptionofmercuryinthefluegasofsewagesludgeincineration.ChemEngJ2003;96:197-205.
doi:10.1016/j.cej.2003.08.018.
[8]GrabowskiZ.IncinerationofsewagesludgebasedonSTUOKrakow.FourthForumofthesludgemanagement2011.
[9]CyrM,CoutandM,ClastresP.Technologicalandenvironmentalbehaviourofsewagesludgeash(SSA)incement-basedmaterials.CemConcrRes2007;37:1278-1289.doi:10.1016/j.cemconres.2007.04.003.
[10]RudnickR,GaoS.Compositionofthecontinentalcrust.In:Rudnick,R.L.(Ed.),TheCrust.In:Holland,H.D.,Turekian,K.K.(Eds.),TreatiseonGeochemistry,vol.3.Elsevier–Pergamon,Oxford;2003,p.1-64.
[11]ZhangF-S,YamasakiS,KimuraK.RareearthelementcontentinvariouswasteashesandthepotentialrisktoJapanesesoils.EnvironInt2001;27(5):393-398.doi:10.1016/S0160-4120(01)00097-6.
[12]Ratafia-BrownJA.Overviewoftraceelementpartitioninginflamesandfurnacesofutilitycoal-firedboilers.FuelProcessTechnol1994;
39:139-157.doi:10.1016/0378-3820(94)90177-5.

[13]WangW,QinY,WangJ,LiJ,WeissDJ.Apreliminarymethodfordeterminingacceptabletraceelementlevelsincoal.Energy2010;35:70-76.doi:10.1016/j.energy.2009.08.028.
[14]LenntechPeriodictable.http://www.lenntech.com/Data-sheets/Periodic-table-chart-of-all-chemical-elements.pdf.
[15]CorellaJ,ToledoJM.Incinerationofdopedsludgesinfluidizedbed.Fateandpartitioningofsixtargetedheavymetals.I.Pilotplantusedandresults.JHazardMater2000;B80:81-105.doi:10.1016/S0304-3894(00)00280-6.
[16]Wilczyńska-MichalikW,MorylR,SobczykJ,MichalikM.Compositionofcoalcombustionby-products:Theimportanceofcombustion
technology.FuelProcessTechnol2014;124:35-43.doi:10.1016/j.fuproc.2014.02.016.
[17]Mardon,SM,HowerJC.Impactofcoalpropertiesoncoalcombustionby-productquality:examplesfromaKentuckypowerplant,IntJCoalGeol2004;59:153-169.doi:10.1016/j.coal.2004.01.004.
[18]ElledAL,AmandLE,LecknerB,AnderssonBA.2007.Thefateoftraceelementsinfluidisedbedcombustionofsewagesludgeandwood.
Fuel2007;86:843-852.doi:10.1016/j.fuel.2006.08.014.
[19]VandeVeldenM,DewilR,BaeyensJ,JossonL,LanssensP.Thedistributionofheavymetalsduringfluidizedbedcombustionofsludge(FBSC).JHazardMater2008;151(1):96-102.doi:10.1016/j.jhazmat.2007.05.056.