Catal Lett (2016) 146:1991–2000 DOI 10.1007/s10562-016-1830-6
N-Hydroxyphthalimide Immobilized on Poly(HEA-co-DVB) as Catalyst for Aerobic Oxidation Processes
Piotr Łątka1· Kornela Kasperczyk2· Beata Orlińska2· Marek Drozdek1·
Bożena Skorupska3· Ewa Witek1
Received: 30 May 2016 / Accepted: 27 July 2016 / Published online: 22 August 2016
© The Author(s) 2016. This article is published with open access at Springerlink.com
AbstractIn the presentstudy,poly(HEA-co-DVB) was synthesized (loading of OH groups: 8.07 mmol OH/g, crosslinking degree: 6 % DVB) and used forN-hydroxyphthalimide (NHPI) immobilization via ester bond (NHPI loading: 2.06 mmol NHPI/g). The obtained polymeric support and poly(HEA-co-DVB)/NHPI cata- lyst were characterized byFT-IRand XPS spectroscopy, elemental analysis, thermogravimetry and particle size measurement. The novel polymer-supported NHPIcatalyst
was tested in aerobic oxidation of p-methoxytoluene and α-methylstyrene. The studied reactions were carried out in the presence of AIBN and/or Co(II) salt without solvent or in acetic acid as solvent. It was found that the obtained polymer-supported NHPI catalyst showed the best cata- lytic performance, which was attributed to a high content ofaccessibleNHPImoieties.Therecoveryandrecyclingof the obtained HEA/DVB-NHPI was only possible in reac- tions proceeded in solvent-freeconditions.
�
Piotr Łątkapiotr.latka@uj.edu.pl
1
FacultyofChemistry,JagiellonianUniversity,Ingardena3, 30-060Kraków,Poland
Department of Chemical Organic Technology and Petrochemistry, Silesian University of Technology, Krzywoustego 4, 44-100 Gliwice, Poland
Institute of Non-ferrous Materials, Mineral Processing and Waste Utilization Department, Sowińskiego 5,
44-100 Gliwice, Poland
2
3
13

1992
P. Łątka et al.
Graphical Abstract
obtained in the presence of Amoco catalyst at significantly higher temperature (190 °C, 1.5 MPa). The role of transi- tion metal salts is initiation of reaction by PINO generation as well as catalyzing the decomposition of formed peroxycompounds into stable products as shown in reactions Eqs.2and6[18]. Metal-free additives, such as azo-compounds, peroxides and aldehydes, act only as initiators and impact on the PINO generation.
KeywordsImmobilizedN-hydroxyphthalimide · Poly(HEA-co-DVB) · Hydrocarbon oxidation
1 Introduction
N-hydroxyphthalimide (NHPI) has been known as a valu- able catalyst for aerobic oxidation of various organic com- pounds [1–3]. Its catalytic effect has been demonstrated among others in oxidation of alkylaromatics, such as tolu- ene, ethylbenzene, cumene and their derivatives, to respec- tive alcohols, ketones, carboxylic acids or hydroperoxides. Recently NHPI was also applied as catalyst for oxidative cleavage of α-methylstyrenes [4]. The activity of NHPI is related to formation of phthalimideN-oxyl radical (PINO) that abstract hydrogen from substrate as shown in Scheme1[5]. Rate of H-abstraction by PINO is higher than by per- oxyl radical in autocatalytic oxidation [e.g. rate constants forH-abstractionfromtoluenebyPINOandROO·are0.08 and 0.21 (mol−1s−1) at 25 °C, respectively] [6]. Addition- ally the catalytic effect is a result of the lower termination rate because of ROO· radicals’ reaction with NHPI inplace and of their recombination to stableproducts.
PINO formation is usually facilitated by additives such as: transition metals [7,8], azo-compounds [9–11], perox-
ides [12,13], aldehydes [14], enzymes [15,16] and others
[17]. For instance, when the most popular combination,
i.e. NHPI and Co(II) salt, was applied in toluene oxidation with oxygen, benzoic acid was obtained in yield of 81 % at25°C(0.1MPa,20h)[18].Inindustry,benzoicacidis
O
2
(1)
II
III
.
Co→CoOO
CoIIIOO.+NHPI→CoIIIOOH+PINO
(2)
Scheme 1Mechanism of hydrocarbon oxidation in the presence of NHPI [5]
13

N-Hydroxyphthalimide Immobilized on Poly(HEA-co-DVB) as Catalyst for Aerobic Oxidation Processes
1993
(3)
Ar−CH3+PINO→Ar−CH.+NHPI
dimensions. The pendant functional groups
are used for
2
the formation of stable covalent bonds with molecules of a catalyst. The pendant functional groups in commercially availablepolystyrenes,suchasNH2andOH,havebeen
previously used by us to immobilize trimellitic anhydride
acid chloride(TAC),which is the precursor of NHPI [22].Nevertheless, commercially available polymers contain only small amount of these functional groups. In the poly-meric beads based on cross-linked 2-hydroxyethylacrylate (HEA), containing high density of hydroxyethyl groups can be employed to immobilize of NHPI via ester bonds. 2-Hydroxyethylacrylate (HEA) is the closest analogue of 2-hydroxyethylmethacrylate (HEMA). Vinyl monomers are also commercially available and are commonly used for synthesis of three-dimensional hydrophilic copolymer networks called hydrogels, synthesized via three-dimen- sional free-radical polymerization (TFRP) [34]. Hydrogels HEMA and HEA-based, due to good mechanical proper- ties, no cytotoxicity, biocompatibility and high thermal stability are applied as biomaterials and coatings [35–39].In particular, the HEMA is the subject of numerous origi- nal papers and monographs on the synthesis,properties and applications of HEMA-based hydrogels, such as the reviewed article of Montheard et al. [40]. The first and the most spectacular application of HEMA-based hydro- gels are soft contact lenses developed by Otto Wichterle in 1960 [41–44]. The immobilization of NHPI on the poly- mer carriers based on HEMA and HEA is not reported in literature, but HEMA-based polymers have been used to immobilize the enzymes [45–47]. Three-dimensional, free- radical copolymerization of HMA and HEA with divinyl monomers called cross-linkers can be carried out using a variety of techniques: bulk cross-linking copolymerization[39,48], solution cross-linking copolymerization [49,50]and suspension cross-linking copolymerization [51]. They showed that HEMA-based hydrogel cross-linked of divi- nylbenzene (DVB) was the smallest deformable polymer tested in this study and had the highest value ofYoung’smodulus. According to these results, it appears that DVB is the appropriate cross-linker for the synthesis of HEA- based carrier to immobilizeNHPI.
In this paper, the application of poly(HEA-co-DVB) as support for NHPI has been reported for the first time. In contrary to previously reported the polystyrene-sup- ported NHPI [22] and GMA/MMA-supported NHPI [23], the new catalyst HEA/DVB-NHPI is characterized by higher NHPI loading. The formed linker is longer than in polystyrene and similar to GMA/MMA supported N– OH groups. There is no data on NHPI loading in other described chemically immobilized NHPI [20,21,24].Herein, activity of this new solid HEA/DVB-NHPIhasbeen studied in oxidation reactions ofp-methoxytoluene andα-methylstyrene.
O2
Ar−CH.→Ar−CH OO.
(4)
2
2
Ar−CH2OO.+NHPI→Ar−CH2OOH+PINO
(5)
CoII+Ar−CH2OOH→→CoIII+Ar−CH2OOH
(6)
Recently, much attention has been paid to heterogeneous catalysts. Application of both immobilized NHPI and metal co-catalyst or combination of homogeneous NHPI and immobilized transition metal co-catalysts has been reported. These catalytic systems are especially attrac- tive due to simple separation from the reaction mixture. Examples of heterogeneous NHPI catalysts include NHPI immobilized on silica gel by physical interaction [19], NHPI immobilized by chemical bonds on silica gel [20,21], polystyrene [22], copolymer microspheres of glycidyl and methyl methacrylate (GMA/MMA) [23] or glycidoxy- propyl-SBA-15 [24] and NHPI incorporated into metal organic framework [25–29]. On the other hand, silica sup- ported cobalt(II) [30,31], cobalt and manganese supported hexagonal mesoporous silicas [32] or cobalt Shiff base complex anchored on starch-coated magneticnanoparticles
[33] were also examined in the presence of homogeneous
NHPI. The activity of these catalytic systems was dem- onstrated in aerobic oxidations of cyclohexane and other cyclic hydrocarbons [19,25,27–29,32], toluenes [20–22,
24], ethylbenzenes [23,25,30,31,33], styrenes [26] as well as other alkyl aromatic compounds [29,31,33] and benzylic alcohols [33]. For example, when toluene was oxidized with oxygen in the presence of both NHPI and Co(II) chemically bonded to silica gel in AcOH as solvent, conversion of 18 % was achieved (100 °C, 0.1 MPa, 20 h)[20]. Similar conversion was obtained when toluene was oxidized under pressure of oxygen in the presence ofN,N- dihydroxypyromellitimide (NDHPI) supported on glyc- idoxypropyl-SBA-15 in MeCN (Co(II), 70 °C, 1.6 MPa, 7 h) [24]. When NHPI immobilized on commercial poly- styrene via amide or ester bonds was applied inp-methoxy- toluene oxidation with oxygen in AcOH or solvent-free condition conversions of 18 and 2.3 %, respectively, were achieved (Co(II), 80 °C, 0.1 MPa, 6 h) [22]. The final effect of NHPI immobilization on a solid carrier by means of covalent bond depends on quantity, quality and distribu- tion of functional groups in a carrier. The cross-linked and thus insoluble synthetic functional polymers are attractive as solid carriers for catalysts and biocatalysts, because they can be formed into grains of predetermined shapeand
13

1994
P. Łątka et al.
2 Experimental

2.1 Materials
deleted the duplicate references and renumbered accord- ingly. Please check and confirm.Now is ok
FT-IR of HEA/DVB: 3392, 2947, 2877, 1721, 1448,
1393, 1239, 1239, 1159, 1073, 888, 841, 756, 741 cm−1.
Elemental analysis of HEA/DVB: C 54.12 %, H 7.13 %, another 38.75 %.
2-Hydroxyethylacrylate
(HEA, 96 %, Aldrich), divi-
nylbenzene (technical 55 %, Sigma–Aldrich), benzoyl peroxide (75 %, Sigma–Aldrich), trimellitic anhydride chloride (98 %, Sigma–Aldrich), hydroxylamine hydro- chloride (98 %, Sigma–Aldrich)N-Hydroxyphthalimide (97 %, Sigma–Aldrich), 2,2′-azobis(2-methylpropionitrile) (AIBN, 98 %, Acros Organics), Co(OAc)2·H2O (pure p.a.,
POCH),were used as received. Solvents Dichloromethane
(DCM, Pure p. a., POCH), Pyridine (Pure p. a., POCH),N,N-dimethylformamide(DMF,Purep.a.,POCH),tetrahy- drofuran(THF,Pure p. a., POCH), diethyl ether (Et2OPure
p. a., POCH), methanol (MeOH Pure p. a., POCH), dichlo-
roethane (DCE Pure p. a., POCH), acetic acid (AcOH, Pure p.a., POCH), acetonitrile (MeCN, pure p. a., POCH). Reagents were used as received without further purifica- tion. Solvents used in catalytic tests such asp-methoxy- toluene (99.8 %, Acros Organics), α-methylstyrene(98 %,
2.2.2 Immobilization of Trimellitic Anhydride Chloride
The mixture of copolymer poly(HEA-co-DVB) (1.00g),DCM(30mL)andpyridine(0.83mL,10mmol)wascooledto 0 °C in ice bath.Next, solutionofTAC(2.17 g, 10mmol) in 30 mL DCM was added dropwise over 1 h. The reaction mixture wasstirredfor 3 h at 0 °C and for additional 24 hatRT.Theproductwasfilteredandwashedtwicewith10mLofsolventin thefollowingorder:DCM,DMF,THF,DCMandEt2O.Product-copolymerpoly(HEA-co-DVB)withimmobi-
lizedTAC(HEA/DVB-TAC)wasdriedundervacuum.Next,
HEA/DVB-TACwas added to a 40 mL mixture ofpyridine: DCE(3:1,v/v),followedby the addition of hydroxylamine hydrochloride (0.71 g, 10 mmol). The mixture wasstirredfor 24 h at 75 °C. The product wasfilteredandwashedwith
Sigma–Aldrich) were purified methods.
and
dried
with
standard
H2O (2×10 mL), MeOH (2×10 mL),
DMF (2×10 mL),
DMF/water (1:1, v/v, 2×10 mL), DMF (1×10 mL), THF
2.2 Preparation of Catalyst
(3×10 mL), DCM (2×10 mL), and Et2O (2×10 mL) and
dried under vacuum. Copolymer poly(HEA-co-DVB) with
immobilized NHPI (HEA/DVB-NHPI) was obtained.
FT-IRofHEA/DVB-TAC:2950, 1852, 1777, 1725,
1456, 1296, 1266, 1228, 1166, 1102, 930, 888, 786, 717,
695 cm−1. Elemental analysis ofHEA/DVB-TAC:C 53.81%,H4.89%,another41.30%.
FT-IR of HEA/DVB-NHPI: 3218, 2937, 1785, 1725,
1454, 1336, 1292, 1253, 1185, 1159, 1104, 1062, 989, 921,
882, 770, 706 cm−1. Elemental analysis of HEA/DVB-
NHPI: C 56.13 %, H 4.91 %, N 2.89 %, another 36.07 %.
Swelling ratio of HEA/DVB-NHPI was determined at
8.4 % in AcOH as a solvent, while there was no swelling of
2.2.1 Polymerization of 2-Hydroxyethylacrylate withDivinylbenzene
Copolymer of HEA and DVB (poly(HEA-co-DVB)) was prepared by mixing HEA (3.00 mL, 26 mmol) and DVB (0.40 mL, 1.54 mmol), then BPO was added (0.48 g, 2mmol).Thesolutionwastransferredintoa30mLvial.The vialwasflushedwithargonandsealed.Thevialwasheated at 60 °C for 6 h. The copolymer was removed from vial, crushed, washed with DCM and dried under vacuum.As references[17],[55]and[39],[49]areduplicate,wehave
Fig. 1Particle size distribution of HEA/DVB-NHPI
13

N-Hydroxyphthalimide Immobilized on Poly(HEA-co-DVB) as Catalyst for Aerobic Oxidation Processes
1995
polymerinp-methoxytolueneandα-methylstyreneobserved. Particle size was measured and mean size was 143 μm (D[3,4]), distribution of particles was in the range between 56.7 and 255.8 μm (d(0.1): 56.667 μm; d(0.5): 124.8μm;
d(0.9):255.8μm)(Fig.1).Specificsurfaceareaofobtained catalyst was 0.0721m2/g.
I.
II.
2.3 Typical Procedure for Oxidation Without Solvent
III.
The oxidation reactions were performed in a gasometric apparatusdescribedinRef.[52].p-Methoxytoluene(2.0mL,
15.9mmol)orα-methylstyrene(2.0mL,16.3mmol),HEA/ DVB-NHPI(0.10g),AIBN(0.03mmol)and/orCo(OAc)2· H2O (0.02 mmol) were placed in a flask connected to agas
burette filled with oxygen under atmospheric pressure. The
mixture was heated up to reaction temperature and stirred at 1400 rpm for 6 or 15 h. The oxygen uptake was mea- sured and recalculated to the conditions of 0 °C and 1 atm. After the reaction, the catalyst was separated through filtra- tion,washedwithMeCNandDCMandthenrecycled.After recycling HEA/DVB-NHPI was characterized byFT-IR.The oxidation products were determined by GCanalysis.
3500 3000
1500
Wave number [cm-1]
1000
Fig. 2FT-IR spectra of HEA/DVB (I), HEA/DVB-TAC (II) and HEA/DVB-NHPI (III)
250 °C. The detector temperature was 280 °C. The tem- perature program was: hold at 50 °C for 5 min, ramp at 5 °C min−1to 200 °C, then ramp at 25 °C min−1to 300 °C for 5 min. Conversion and selectivity were calculatedbasedon internal standard-cyclohexanone. GC analysis of prod- ucts of α-methylstyrene oxidation was performed using a Hewlett 5890 Series II Gas Chromatography (Zebron ZB- 5HT capillary column, 30 m×0.32 mm×0.1 µm, helium 48 kPa) with FID detector. The injection port temperature was 280 °C. The detector temperature was 280 °C.The temperature program was: hold at 70 °C for 2 min, ramp at 5°Cmin−1to100°C,thenrampat20°Cmin−1to250°Cfor 2 min. Conversion and selectivity were calculated based oninternalstandard-naphthalene.
Thermogravimetric analysis (TG) was carried out in SDT q600 thermobalance(TAinstrument). The measure- ment was performed in corundum crucibles using about 10 mg of sample. The decomposition of the organic part was monitored in an air flow (100×mL/min) while the temperature was increased from 30 to 1000 °C at a rate of 20 °C min−1. Particle size and surface area were measured on MASTERSIZER 2000MALVERNINSTRUMENTS.
2.4 Typical Procedure for Oxidation in AcOH
p-Methoxytoluene(0.63mL,5mmol),AcOH(10mL),HEA/ DVB-NHPI (0.10 g), cobalt(II) acetate(Co(OAc)2⋅H2O,
0.02 mmol) and AIBN (0.03 mmol) were placed in a flask
connected to a gasometric apparatus. Reaction was con- ducted at 80 °C for 6 h. The oxidation procedure was the same as for the oxidation described above.
2.5 Analytical Methods
Infrared spectra were recorded on a Nicolet 6700FT-IRSpectrometer.ElementalanalysiswasperformedonaCHNSVarioMicro Cube. GC analysis of products ofp-methoxy- toluene oxidation was performed using an AgilentTech-nologies 7890A/5975C Gas Chromatography (HP-5 MS capillarycolumn,30m×0.25mm×0.25µm,helium1.2mL/ min) with FID detector. The injection port temperature was
The
X-ray
photoelectron
spectra
(XPS)
were acquired
Scheme 2Immobilization ofN-hydroxyphthalimide on synthesized copolymer poly(HEA-co-DVB)
OH
O
O
O
BPO
O
O
O
TAC
NH2OH HCl
+
O

80 °C,24 h
0 °C,24 h
75°C,24 h
O
HEA
OH
O	O
O
O
DVB
HEA/DVB
O
O
O
HEA/DVB-TAC
NOH
HEA/DVB-NHPI
O
O
13

O-H	O=C(O)

O=C(O)	O=C(O)
(O)C-O

(N)O-H	O=C(N)	O=C(O)(O)C-O

1996
P. Łątka et al.
3.1 Preparation of Catalyst
(C=O)2N-OH
N 1s
Copolymer poly(HEA-co-DVB) was synthesized by polymerization of HEA and DVB, then NHPI was immo- bilized on prepared HEA/DVB as shown in Scheme2. TheFT-IRspectrum (Fig.2I) of HEA/DVB showed character- istic peaks of hydroxyl and carbonyl groups at 3392 and 1721 cm−1, respectively. After immobilization ofTAC,the peak of hydroxyl group at 3392 cm−1disappeared onFT-IRspectrum (Fig.2II). TheFT-IRspectrum of Fig.2II.
NHPI

HEA/DVB-NHPI
cm−1
showed new peaks at 1852 and 1777
correspond-
ing to anhydride groups [53] and 1228 cm−1—stretching
vibrations of C–O bond. The appearance of new anhydride bonds as well as disappearance of hydroxyl group bond confirmed immobilization ofTAC. FT-IRspectrum of final
406
404
402
400
398
396
Binding Energy (eV)
Fig. 3N 1s DVB-NHPI
high-resolution
XPS
spectra
of
NHPI
and
HEA/
cm−1
product—HEA/DVB-NHPI showed peak at 3218
(Fig.2III) corresponding to hydroxyl group in obtainedN-hydroxyphthalimide moiety. Moreover, characteristic bond of anhydride group at 1852 cm−1disappeared and car-
using a Prevac photoelectron spectrometer equipped with a hemispherical VGSCIENTAR3000 analyzer. The spec- tra were taken using a monochromatized aluminum source AlKα(E=1486.6eV)andalow-energyelectronfloodgun (FS40A-PS) to compensate for the charge accumulation on the surface of nonconductive samples. Spectra were pro- cessed and deconvoluted using CasaXPSsoftware.
bonyl bond at 1777 cm−1(O=C(O)) shifts to 1785 cm−1(O=C(N)).Peaksat3218and1785cm−1confirmedforma- tion ofN-hydroxyl group and obtaining immobilized form ofN-hydroxyphthalimide [17,54].
TheXPSanalysiswasperformedtoconfirmthepresence of catalytic centers on the surface of material. ThepresenceofN1speakinobtainedcatalystconfirmedtheimmobiliza- tion of NHPI onto polymeric support. The high-resolution N 1 s spectra collected for NHPI as well as for HEA/DVB- NHPI are displayed on Fig.3. The N 1 s core level spectra were fitted with only one component. In the case of NHPI binding energy of N–OH is 401.4 eV and in HEA/DVB- NHPI binding energy of N–OH group is 401.5eV.
3 Results and Discussion
In this paper, new polymer—supported NHPI was obtained and examined in selected oxidation reactions. Copolymer poly(HEA-co-DVB) was used to immobilized NHPI via ester bond.
Fig. 4Thermogravimetric spectrum of HEA/DVB-NHPI
0,6
100
80
0,4
60
40
0,2
20
0
0,0
0
200
400
600
800
1000
Temperature (°C)
13
Intensity (a.u.)
Weight (%)
Deriv, Weight (%/°C)

N-Hydroxyphthalimide Immobilized on Poly(HEA-co-DVB) as Catalyst for Aerobic Oxidation Processes
1997
Table 1Oxidation ofp-methoxytoluene in the presence of HEA/DVB-NHPI
p-Methoxytoluene
Entry
Temperature (°C)
Time (h)
Co(OAc)2·H2O (mmol)
HEA/DVB-NHPI
O2consumed (mmol)
mmol
mL
Recycle
g
1
2
3
4
5
6
7
8
9
10
11
12
13
14
15
16
17
18
19
20
21
22
23
24
25
5.0a
5.0a
5.0a
5.0a
15.9
15.9
15.9
15.9
15.9
15.9
15.9
15.9
15.9
15.9
15.9
15.9
15.9
15.9
15.9
15.9
15.9
15.9
15.9
15.9
15.9
0.63
0.63
0.63
0.63
2.0
2.0
2.0
2.0
2.0
2.0
2.0
2.0
2.0
2.0
2.0
2.0
2.0
2.0
2.0
2.0
2.0
2.0
2.0
2.0
2.0
80
80
80
80
70
70
70
80
80
80
80
80
80
80
80
80
80
80
80
80
80
90
90
90
90
6
6
6
6
6
6
6
6
6
6
6
6
6
6
6
6
6
6
6
15
15
6
6
6
6
0.02
0.02
0.02
0.02
0.02
0.02
0.02
0.0
0.0
0.02
0.02
0.02
0.02
0.02
0.02
0.02
0.02
0.02
0.02
0.02
0.02
0.02
0.02
0.02
0.02
– 0
1
2
– 0
1
– 0
– 0
0
0
0
– 0
1
2
3
– 0
– 0
1
2
– 0.10
0.10
0.08
– 0.10
0.09
– 0.10
– 0.025
0.05
0.10
0.15
– 0.10
0.09
0.09
0.08
– 0.10
– 0.10
0.10
0.09
0.02
3.33
0.25
0.00
0.04
0.14
0.13
0.03
0.12
0.04
0.06
0.09
0.17
0.11
0.04
0.17
0.62
0.47
0.48
0.71
1.01
0.92
1.34
0.93
0.80
HEA/DVB-NHPI (0.206 mmol of NHPI), AIBN (0.03 mmol), 1 atm, 1400 rpm
aReaction in AcOH (10 mL)
Based on elemental analysis, loading of hydroxyethyl groups in HEA/DVB and cross-linking degree were calcu- lated as 8.07 mmol OH/g and 6 % DVB, respectively. The results of elemental analysis were also used to calculate NHPI loading of 2.06 mmol NHPI/g.
LoadingofimmobilizedNHPI waslowerthanexpected basedonhigh amountof –OHloadingin synthe- sized support. However, NHPIloadingandcross-linkingdegreeof HEA/DVB-NHPI werehigherincomparisonto reported NHPI supported oncommerciallyavailable(chloromethyl)polystyrene viaester bond(maximumloading 1.65 mmolNHPI/g,maximumcross-linkingdegree5.5 % DVB)[22].Incontraryto ourobtainedheterogeneousNHPI, GMA/MMA-NHPImicrosphereswerecharacterizedbylower amountof NHPIpreviouslybonded througha Schiffbasereaction(1.1 mmol/g)andethylene glycol dimethacrylateascross-linker(nodataofcross-linking degree) [23]. Thereis nodataon NHPIloadinginother described chemically immobilizedNHPI[20,21,24].
Stability of polymer was investigated by Thermogravi- metric analysis (Fig.4). TG spectra can be distinguishedby tworegionsofmassloss:(I)upto150°Cwhichcorrespond- ing to physically adsorbedwater,(II) above 150 °C which corresponding to desorption and oxidation of material. Three stages of weight loss in TG curve over 150 °C were observed: (a) area of 150–250 °C showed start of catalyst decomposition, (b) area between 250 and 500 °C showed major weight loss which were characteristic for carboniza- tion of sample and c) area above 500 °C was characterized as carbon oxidation. TG analysis demonstrated stability of obtained immobilized NHPI in temperature of performed oxidation reactions.
3.2 Catalytic Tests of HEA/DVB-NHPI
p-Methoxytoluene and α-methylstyrene were used as start- ing material for catalytic tests of obtained new polymer- supported NHPI. Oxidation of model compounds was performedinthepresenceofHEA/DVB-NHPIbothinpolar
13

1998
P. Łątka et al.
Table 2Oxidation of α-methylstyrene in the presence of HEA/DVB- NHPI
I.
(O)C-O
Entry
Tem- pera- ture (°C)
Time (h)
Co(OAc)2·H2O
(mmol)
HEA/DVB-NHPI
O2
con-
sumed (mmol)
II.
Recycle
g
O-H
III.
1
2
3
4
5
6
7
8
9
10
11
14
70
70
70
70
70
70
80
80
80
80
80
80
6
6
6
6
15
15
6
6
6
6
6
6
0.0
0.0
0.0
0.0
0.0
0.0
0.0
0.0
0.0
0.0
0.02
0.02
– 0
1
2
– 0
– 0
1
2
–
2
– 0.10
0.10
0.10
– 0.10
– 0.10
0.10
0.09
– 0.09
3.4
4.6
5.7
5.4
6.6
8.3
5.1
5.5
5.8
4.0
5.1
4.9
(N)O-H
O=C(N)
O=C(O)
(O)C-O
4000
3500
3000
2500
2000
1500
1000
Wave number [cm-1]
Fig. 5FT-IR spectra of
fresh HEA/DVB-NHPI (I), reused HEA/
DVB-NHPIinAcOH(II)andreusedHEA/DVB-NHPIinsolvent-free system(III)
conditions that could abstract hydrogen mainly fromNHPI. For instance, whenp-methoxytoluene was oxidized in the presenceofHEA/DVB-NHPIandCo(II)saltwithoutAIBN, indication period of 30 min was observed at 80 °C. It was reduced to 9 min after AIBN addition. Effect of Co(II) salt in oxidation of bothp-methoxytoluene andα-methylstyrene in the presence of HEA/DVB-NHPI was studied. When reaction ofp-methoxytoluene withHEA/DVB-NHPI/
Co(II) system was performed the higher O2consumption were achieved (Table1, entries 9, 16). Additionally, induc-
tion period was reduced from 14 to 7 min. In oxidation of α-methylstyrene similar oxygen consumption was obtained inthepresenceofHEA/DVB-NHP/Co(II)systemandwith- out additive of metal salt(Table2, entries 8, 12).Similarly,no effect of Co(II) salt additive on NHPI-catalyzed oxida- tion of α-methylstyrene was reported in paper[4].
The higher catalytic effect of HEA/DVB-NHPI was observed in oxidation ofp-methoxytoluene than α-methylstyrene. For example, consumption of O2in
α-Methylstyrene (2 mL, 16.3 mmol), HEA/DVB-NHPI (0.206 mmol
of NHPI), AIBN (0.03 mmol), 1 atm, 1400 rpm
solventaswellasinsolvent-freeconditions.Reactionswere performed at temperature in the range of 70–90 °C in the presenceofAIBNorAIBNandCo(II)salt.Oxygenuptakes were used to observe reactions progress and were collected inTables1and2. Immobilized NHPI was recycled up to three times. Inconsiderable loss of catalyst during filtration was observed due to small mesh size of catalyst and low scale of performedoxidation.
It was proved that obtained HEA/DVB-NHPI could successfully catalyzed oxidation processes ofp-methoxy- toluene and α-methylstyrene in solvent-free conditions. Studied reactions were performed in the presence of AIBN or AIBN/Co(II) system. AIBN was added in the amount of 0.1–0.2 mol% in order to initiate the oxidation process and reduce the induction period. AIBN decomposed to alkyl radicals (2-cyanoprop-2-yl radicals) under theapplied
p-methoxytoluene
at
80 °C increased up to 15.5 times
Table 3Composition of oxidation products ofp-methoxytoluene and α-methylstyrene
Conversionc(%)
Selectivityc(%)
Entry
Substrate
HEA/DVB-NHPI (g)
Aldehyde
Alcohol
Acid
1
2
p-Methoxytoluenea
–
0.1
3.8
4.9
44
46
Acetophenone 73
66
37
31
19
23
α-Methylstyreneb
3
4
–
0.1
61
70
ap-Methoxytoluene(2 mL, 15.9 mmol), Co(OAc)2·H2O (0.02 mmol), AIBN (0.03 mmol), 80 °C 1 atm, 1400 rpm, 15 h
bα-Methylstyrene (2 mL, 15.9 mmol), AIBN (0.03 mmol), 70 °C 1 atm, 1400 rpm, 15 h
cBased on GC analysis
13

N-Hydroxyphthalimide Immobilized on Poly(HEA-co-DVB) as Catalyst for Aerobic Oxidation Processes
1999
O=C(O) at 1725 cm−1and O=C(NOH) at 1785 cm−1was not changed. Furthermore, peak at 3218 cm−1characteristic forN-hydroxyl group was strengthened.
The composition of products obtained in oxidation ofp-methoxytoluene and α-methylstyrene was determined by GC-FID analysis and presented in Table3.p-Methoxytolu- ene was oxidized top-methoxybenzaldehyde,p-methoxy- benzyl alcohol andp-methoxybenzoic acid while main product of α-methylstyrene oxidation was acetophenone.
(Table1, entry17) in comparison to reaction performed without HEA/DVB-NHPI(Table1, entry 15). As expected, therateofoxidationreactionofα-methylstyrenewashigher thanp-methoxytoluene. However, the increased of O2con- sumption was lower, for example at 70 °C increased only up to 1.7 times(Table2, entry 3) in comparison to reaction without NHPI(Table2, entry 1).
The catalytic activity of immobilized NHPI was simi- lar in subsequent recycles(Table1, entries 16–19;Table2, entries 2–4), which could prove stability of novel hetero- geneous organocatalyst at the temperatures up to 80 °C. It was observed that catalytic activity of recycled immobi- lized NHPI was sometimes higher than the freshone’s.It is assumed that groups presented in solid catalyst that inhibit free radical reaction could be oxidized to inactive oncedur- ing firstusage.
The effect of temperature on oxidation ofp-methoxy- toluene and α-methylstyrene in the presence of HEA/ DVB-NHPI was also examined. As expected, the oxygen uptake increased when temperature rose. However, the O2
consumption in comparison to blank reaction was lower at
90°C(1.45times)thanat80°C(4.25times)forp-methoxy- toluene and at 80 °C (1.1 times) than 70 °C (1.3 times) for α-methylstyrene.Itshowsthattherateofnon-catalyticreac- tions is higher at the higher temperature.
The effect of amount of immobilized NHPI was stud- ied in oxidation ofp-methoxytoluene. HEA/DVB-NHPI at amount of 0.025, 0.05 and 0.15 g caused lower catalytic effect than 0.1 g. An excessive amount of heterogeneous NHPI(0.15g)inrelationto2mLofreactionmixturecaused worst effectiveness resulted in lower consumption ofO2.
ObtainedHEA/DVB-NHPIwasalsousedinoxidationof
p-methoxytolueneperformedinaceticacidasapolarsolvent(Table1, entries 2–4). Previously reported NHPI immobi- lized on polystyrene by amide or ester bonds demonstrated significantly higher activity in the presence of polarsolvent but the activity was lost during recycles [22]. It seemed that higher cross-linked novel HEA/DVB-NHPI would be more stable in solvent conditions. Over 160 times higher oxygen consumption in the process with novel heteroge- neous NHPI than in oxidation without NHPI was observed. Unfortunately,catalyticactivityofreusedHEA/DVB-NHPI significantlydecreased.FT-IRanalysisofHEA/DVB-NHPI after second recycle in the solvent conditions (Fig.5II) showed decreasing of the intensity of peaks at 1785, 1785 and 1159 cm−1assigned to the carbonyl group (O=C(N– OH)) and ester bonds –C–O– (both in immobilized NHPI and in copolymer poly(HEA-co-DVB)). The signal of hydroxylgroupat3392cm−1,presentedinHEA/DVBspec-
trum (Fig.1I) beforehand, was observed. Cleavage of the
ester bonds in heterogeneous NHPI occurred in contrast to HEA/DVB-NHPI after second recycle in solvent-free sys- tem (Fig.5III). Intensity of both signals of carbonyl groups
4 Conclusion
This paper shows that immobilization of NHPI on copo- lymer poly(HEA-co-DVB) via ester bond has been suc- cessfully achieved. The structure of novel heterogeneous catalystwasconfirmedbyFT-IRandXPSspectroscopyand elemental analysis. Based on the results of elementalanaly- sis the amount of immobilized NHPI and the crosslinking degree of carrier were calculated respectively 2.06 mmol NHPI/g and 6 mol% of DVB. The amount of NHPI immo- bilized on investigated carrier is higher than on commer- cially available polystyrenes (MPS-NHPI: 0.35–1.65 mmol NHPI/g) [22] as well as on copolymer of glycidyl meth- acrylate and methyl methacrylate(GMA/MMA-NHPI:
1.1 mmol NHPI/g) [23]. There is no data about NHPI load- ing of silica-supported NHPI [20,21] and NDHPI immobi- lized on SBA-15 [24]. Additionally, the ester bondbetween activeN-hydroxylgroupandinvestigatedcarrierhasgotthe ethyl-linker, which is longer than in polystyrene-based car- rier[22].
HEA/DVB-NHPI was applied in oxidationp-methoxy- toluene in AcOH as solvent. O2consumption in compari- son to NHPI loading of HEA/DVB-NHPI was 16 mmol
O2/mmol N–OH (Co(II), 80 °C, 1 atm, 5 h). Itwassignifi- cantly higher than in comparison topreviouslyreportedsilica-supportedNHPIandCo(II)saltusedinoxidationof tolueneO2,whenO2uptakeperNHPIloadingwascalcu- lated as only 4.8 mmol O2/mmol NOH (80 °C, 1 atm,20h)[20]. Unfortunately, HEA/DVB-NHPI wasunstablein AcOHduetodegradationoftheesterbondsinacidicmedia. Activity	of	HEA/DVB-NHPI	was	also	demon- strated in oxidation reactions ofp-methoxytolueneand α-methylstyrene in solvent-free system. Whenreactionwascarriedoutwithoutsolventrecoveryandrecyclingofimmo- bilizedNHPIwerepossible.Incomparisontopreviously studiesofchemicallybondedNHPI[20–24],theobtained HEA/DVB-NHPIrepresentedhigheractivitypermoleof immobilizedNHPI.DeterminedamountofO2consumed peramountofimmobilizedNHPIwas3.3mmolO2/mmol N–OHand2.7mmolO2/mmolN–OHinp-methoxy- toluene oxidation in the presence ofnovelHEA/DVB-NHPI (2.06 mmol NHPI/g) and in previouslydescribed
13

2000
P. Łątka et al.
23.
24.
25.
Gao B, Meng S, Yang X (2015) Org Process Res Dev 19:1374 Zhou M, Li X, Bao L, Yuan X, Luo H (2015) Catal Lett 2:383 Dhakshinamoorthy A, Alvaro M, Garcia H (2011) Chem Eur J17:6256
Dhakshinamoorthy A, Alvaro M, Garcia H (2011) ACS Catal1:836
DhakshinamoorthyA,AlvaroM,GarciaH(2012)JCatal289:259 MikamiY,Dhakshinamoorthy A, Alvaro M, Garcia H (2013)Chem Cat Chem 5:1964
Yua P, Liub G, Tangb R (2014) Curr Organocatal 1:79
Rajabi F, Luque R, Clark JH, Karimi B, Macquarrie DJ (2011)Catal Commun 12:510
ChenL,LiB-D,XuQ-X,LiuD-B(2013)ChinChemLett24:849YuaWH, Zhoub CH,TongbDS, Xua TN (2012) J Mol Catal AChem 365:194
Jafarpour M, Rezaeifard A, Yasinzadeh V, Kargar H (2015) RSCAdv. doi:10.1039/C5RA04718H
Matsumoto A (1995) Springer, Berlin Heidelberg pp 41–80 MontheardaJ-P,ChatzopoulosaM,DanielCh(1992)JMacromol Sci Pol R32:1
Horàk D, Jayakrishnan A, Arshady R (2003) In: Arshady R (ed) Polymers in medicine and biology, vol 1. Citus Books, London, pp 80–107
Horàk D (2006) In: Pethrick CA, Zaokov EE (eds) Handbookof polymer research, vol 19. Nova Science Publishers Inc, NewYork,pp1–33
Moghdam MN, Pioletti DP (2015) J Biomed Mater Res Part B00B:000
Meherchi L, Chabane Sari SM, Senoudi AR, Zargou S, Ben-mouna F (2015) J Mater Environ Sci 6:2221
Montheard JP, Chatzopoulos M, Chappard D (1992) J MacromolSci. Macromol Rev 32:1
Wichterle O, Lim D (1960) Nature 185:117Kunzler J, McGee J (1995) Chem Ind 16:651Wichterle O (1972) US Patent 3,679,504
Kopeček J (2009) J Polym Sci A Polym Chem 47:5929
Basri M, Samsudin S, Bin Ahmad M, Razak CNA, Salleh AB (1999) Appl Biochem Biotech 81:205
Ayhan F, Ayhan H, Piskin E, Tanyolac A (2002) BioresourceTechnol 81:131
Hamdy S, El-Sigeny S, Abou TM (2008) J Macromol Sci A45:980
Serrano AA, Campillo Fernàndeza AJ, Gómez Ribellesa JL,Monleón PM, Gallego FG, Pissisb P (2004) Polymer 45:8949MonleónPM,GómezRibellesJL,SerranoAA,GallegoFG,SuayAJ, Pissis P (2001) Polymer42:4667
Santander-Borrego M, Green DW, Chirila TV, Andrew K, Whit-taker AK, Blakey I (2014) J Polym Sci Pol Chem 52:1781
Okay O, Gurun C (1992) J Appl Polym Sci 46:401
Kasperczyk K, Orlinska B, Zawadiak J (2014) Cent Eur J Chem12:1176
Konieczynska MD, Dai C, Stephenson CRJ (2012) Org BiomolChem 10:4509
Krishnakumar V, Manohar S, Nagalakshmi R (2008) Spectro- chim Acta A 71:110
(chloromethyl)polystyrene-supported NHPI (1.65 mmol NHPI/g), respectively, under the same reaction conditions. However, as results of higher loading of NHPI and longer linker, higher oxygen uptake was achieved when HEA/ DVB-NHPI was used.
26.
27.
28.
AcknowledgmentsFinancial assistance from the National Sci- ence Centre of Poland (Grant No. N N209 755440) isgratefully acknowledged. Part of the research was done with equipment pur- chased in the frame of European Regional Development Fund (Polish Innovation Economy Operational Program—contract no. POIG.02.01.00-12-023/08).
29.
30.
31.
32.
Open AccessThis article is distributed under the terms of the Creative Commons Attribution 4.0 International License (http://cre-ativecommons.org/licenses/by/4.0/), which permits unrestricted use, distribution, and reproduction in any medium, provided you give appropriate credit to the original author(s) and the source, provide a link to the Creative Commons license, and indicate if changes were made.
33.
34.
35.
36.
37.
References
38.
1.
2.
3.
4.
5.
Recupero F, Punta C (2007) Chem Rev 107:3800 Coseri S (2009) Cat Rev Sci Eng 51:218
Chen K, Zhang P, Wang Y, Li H (2014) Green Chem 16:2344 Lin R, Chen F, Jiao N (2012) Org Lett 14:4158
AmoratiR,LucariniM,MugnainiV,PedulliGF,MinisciF,Recu- peroF,FontanaF,AstolfiP,Greci L (2003) J Org Chem 68:1747 SheldonRA,ArendsIWCE(2006)JMolCatalA:Chem251:200 AokiY,Hirai N, Sakaguchi S, Ishii Y (2005) Tetrahedron 61:10995
Coseri S (2009) Catal Rev 51:218
Aoki Y, Sakaguchi S, Ishii Y (2004) Adv Synth Cata 346:199 Arends IWCE, Sasidharan M, Kühnle A, Duda M, Jost C, Shel- don RA (2002) Tetrahedron 58:9055
PuntaC,RectorCL,PorterNA(2005)ChemResToxicol18:349TsujimotoS, IwahamaT,Sakaguchi S, Ishii Y (2001) Chem Commun (Camb)22:2352
Tsujimoto S, Sakaguchi S, Ishii Y (2003) Tetrahedron Lett 44:5601
MinisciF,Gambarotti C, Pierini M, Porta O, Punta C, RecuperoF,Lucarini M, Mugnaini V (2006) Tetrahedron Lett 47:1421 d’AcunzoF,BaioccoP,Galli C (2003) New J Chem 27:329 SakaguchiS,EikawaM,IshiiY(1997)TetrahedronLett38:7075YangG, MaY,Xu J (2004) J Am Chem Soc126:10542
YoshinoY,HayashiY,IwahamaT,Sakaguchi S, Ishii Y (1997) J Org Chem 62:6810
Hermans I, Van Deun J, Houthoofd K, Peeters J, Jacobs P A (2007) J Catal 251:204
RajabiF,Clark JH, Karimi B, Macquarrie DJ (2005) Org BiomolChem 3:725
IshiiY,Takano M, Hirai N (2010) US Patent 0317869 KasperczykK,OrlinskaB,WitekE,LatkaP,ZawadiakJ,Pronie- wicz L (2015) Catal Lett145:1856
39.
40.
41.
42.
43.
44.
45.
6.
7.
8.
9.
10.
46.
11.
12.
47.
48.
13.
49.
14.
50.
15.
16.
17.
18.
51.
52.
53.
19.
54.
20.
21.
22.
13