Vol. 50 No. 2/2003
471–479
QUARTERLY
Collagen type II modification by hypochloriteO
S³awomir Olszowski2, Pawe³ Mak3, Ewa Olszowska2 and Janusz Marcinkiewicz1
1Department of Immunology, Collegium Medicum, Jagiellonian University, Kraków, Poland; 2Institute of Medical Chemistry, Collegium Medicum, Jagiellonian University, Kraków, Poland; 3Faculty of Biotechnology, Jagiellonian University, Kraków, Poland
Received: 16 January, 2003; revised: 10 April, 2003; accepted: 20 April, 2003
Key words: collagen, hypochlorite, taurine chloramine, rheumatoid arthritis, oxidative modification
Oxidation of proteins is a common phenomenon in the inflammatory process medi- ated by highly reactive agents such as hypochlorite (HOCl/OCl–) produced by acti- vated neutrophils. For instance, in rheumatoid arthritis hypochlorite plays an impor-
tant role in joint destruction. One of the major targets for HOCl/OCl– is collagen type
II (CII) — the primary cartilage protein. In our study, HOCl/OCl– mediated collagen II
modifications were tested using various methods: circular dichroism (CD), HPLC, ELISA, dynamic light scattering (DLS), fluorimetry and spectrophotometry. It was shown that hypochlorite action causes deamination with consecutive carbonyl group formation and transformation of tyrosine residues to dichlorotyrosine. Moreover, it was shown that ammonium chloramine (NH2Cl) formed in the reaction mixture reacts with CII. However, in this case the yield of carbonyl groups and dichlorotyrosine is
lower than that observed for HOCl/OCl– by 50%. CD data revealed that collagen II ex-
ists as a random coil in the samples and that chlorination is followed by CII fragmenta- tion. In the range of low HOCl/OCl– concentrations (up to 1 mM) 10–90 kDa peptides are predominant whereas massive production of shorter peptides was observed for
high (5 mM) hypochlorite concentration. DLS measurements showed that chlorina- tion with HOCl/OCl– decreases the radius of collagen II aggregates from 30 to 6.8 nm.
Taking into account the fact that chlorinated collagen is partially degraded, the DLS results suggest that smaller micelles are formed of the 10–90 kDa peptide fraction. Moreover, collagen chlorination results in epitope modification which affects CII rec- ognition by anti-CII antibodies. Finally, since in the synovial fluid the plausible hypochlorite concentration is smaller than that used in the model the change of size of molecular aggregates seems to be the best marker of hypochlorite-mediated collagen oxidation.
O
This work was supported by a grant from the State Committee for Scientific Research (KBN, Poland)
grant No. 4P05B01018.

Corresponding author: Department of Immunology, Collegium Medicum, Jagiellonian University,
31-121 Kraków, Czysta 18, Poland; fax: (48 12) 633 9431; e-mail: mmmarcin@cyf-kr.edu.pl
Abbreviations: BSA, bovine serum albumin; CII, collagen type II; HRP, horseradish peroxidase; OPD, o-phenylenediamine dihydrochloride; PMNs, neutrophils; RA, rheumatoid arthritis; ROS, reactive oxy- gen species; TFA, trifluoroacetic acid.

472
S. Olszowski and others
2003
Protein oxidation by reactive oxygen species
(ROS) plays an important role in the patho- mechanism of inflammatory diseases. ROS are produced by neutrophils, the main cells of inflammed synovial fluid in rheumatoid ar- thritis (RA). They are responsible for cartilage damage and joint erosion observed in this dis- ease. The most toxic ROS generated by acti- vated neutrophils is hypochlorite (HOCl/ OCl–) — the product of the myeloperoxi- dase/Cl–/hydrogen peroxide system (Weiss et al., 1982). Collagen type II (CII) is a primary protein component of cartilage and destruc- tion of this protein caused by hypochlorite and by collagenase is one of the principal pathological reactions observed in RA (Ed- wards & Hallett, 1997).
It has been demonstrated (Weiss et al., 1983) that HOCl/OCl– can react rapidly with amino acids and proteins to form low molecular and protein N-mono(di)chloramines. Davies et al. (1993) have shown that hypochlorite action leads to intensive fragmentation of tritiated acid soluble bovine collagen type II and that some of the amino acid-derived chloramines (N-chloroleucine or N-chloroalanine) increase the proteolytic susceptibility of N-chloramine modified collagen. At present, however, the knowledge of the early stages of HOCl/OCl– mediated collagen oxidation is poor. In our study we used various methods to monitor hypochlorite-mediated changes in CII amino- acid residues as well as changes in the struc- ture of this protein.
benzenesulfonic acid, ethanol and ethyl ace-
tate were obtained from Sigma (St. Louis, U.S.A.). 2,4-Dinitrophenylhydrazine was from Merck (Darmstadt, Germany). Sodium hypo- chlorite (NaOCl) and sodium chloride were from Aldrich Chemie (Steinheim, Germany). Taurine, Nessler reagent and trifluoroacetic acid (TFA) were from Fluka Chemica AG (Buchs, Switzerland). Anti-human collagen type II antibody monoclonal purified IgG (clone II 4011) was from ICN Biomedicals, Inc. (U.S.A.). Horseradish peroxidase strepta- vidin was from Vector Lab (Burlingame, CA, U.S.A.). NaOCl solutions were prepared prior to use from 0.57 M stock solution and stan- dardized iodometrically (Stelmaszyñska & Zgliczyñski, 1978).
Ammonium monochloramine synthesis. Two millimolar NH2Cl was prepared prior to use in a cuvette. Forty microliters of 4 mM HOCl/OCl– in 0.2 M phosphate buffer, pH 7.4, was added to 0.96 ml of 4 mM NH4H2PO4 in the same buffer.
Taurine monochloramine synthesis. Taurine monochloramine solutions (1–5 mM) were prepared as follows. One millilitre of 2–10 mM hypochlorite solution in 0.2 M phos- phate buffer, pH 7.4, was added dropwise to 1 ml of 2–10 mM taurine in the same buffer. The final taurine monochloramine concentra-
tion was calculated using E253nm = 0.4 mM–1
X cm–1 (Stelmaszyñska & Zgliczyñski, 1978). Collagen chlorination with HOCl/OCl– (1), ammonium monochloramine (2) or
taurine monochloramine (3).
(1) Samples
of collagen (2 mg/ml) in 0.2 M phosphate
buffer, pH 7.4, with 0.2 M NaCl were incu- bated for 2 h with 1, 3 or 5 mM HOCl/OCl– or
for 30 min with 0.2, 1, 2 or 4 mM HOCl/OCl–. To stop the reaction the samples were treated with a steichiometric amount of thiosulfate (1/1). The dichlorotyrosine, tyrosine and alde- hyde groups were assayed in the samples and additionally in the fractions of molecular mass < 10 kDa.
(2 and 3). Collagen samples (1 mg/ml) in 0.2 M phosphate buffer, pH 7.4, with 0.2 M NaCl
MATERIALS AND METHODS
Chemicals. Collagen type II (CII) from
chicken sternal cartilage, pronase E, biotiny- lated goat anti-mouse IgG antibody, potas- sium hydroxide, acetonitrile, sulfuric acid, hy- drochloric acid, citric acid, sodium mono- and
dihydrophosphate,
ammonium
dihydro-
phosphate, guanidinium hydrochloride, so-
dium thiosulfate, hydrogen peroxide, o-phe- nylenediamine dihydrochloride, 2,4,6-trinitro-

Vol. 50
Collagen type II modification by hypochlorite
473
were incubated with
2 mM ammonium chlo-
formed from 0 to 100% of B within 15 min.
Twenty micrograms of unchlorinated or HOCl-modified collagen was loaded onto the column. (2) Assays were performed using a Shimadzu SCL 10A apparatus equipped with a Supelcosil TM LC-318 C-18 column (4 X 250 mm) and the buffer set as follows: (A) 0.1% TFA in water, (B) 0.1% TFA in acetonitrile. Gradient was formed from 0 to 100% of B within 30 min. One hundred microliters of sample was filtered through a Milipore YM 10 kDa membrane and loaded on to the column. Electrophoresis. SDS/PAGE was per- formed in a MiniProtean II apparatus (BioRad, U.S.A.) using Tris/Tricine protein gels, 3.25 µ g of total protein was loaded into each well. The gels were stained with Cooma- ssie Blue R-250 or silver stained.
Competitive ELISA. To determine collagen epitope modification by chlorination competi- tive ELISA was used. Briefly, microtiter plates (Corning, U.S.A.) were coated with 5
µg/ml of CII. The antigens tested (CII modi- fied by HOCl/OCl– or taurine monochlora- mine) at 0.5–50 µg/ml were mixed with an anti-CII monoclonal antibody (12.5 µg) and then added and incubated with a fixed compet- itive antigen for1h at room temperature and washed 3X to remove nonadsorbed immune complexes. The plates were then incubated with biotinylated goat anti-mouse antibody for 45 min at room temperature. Horseradish peroxidase (HRP) conjugated streptavidin di- luted 1:1000 in 1% BSA/PBS was added and the plates were incubated for 45 min at room temperature. Then o-phenylenediamine dihy- drochloride (OPD) was used as a substrate (5 mg of OPD in 10 ml of phosphate/citrate
ramine or with 1, 3 or 5 mM taurine chlo- ramine for 2 h at 37oC. The progress of reac- tion (2) was monitored by the decrease of ab-
sorption at 253 nm and the resulting NH2Cl concentrations were calculated as above.
Estimation of dichlorotyrosine. Dichloro- tyrosine concentration was calculated from difference spectra of chlorinated collagen (2
mM–1	cm–1
mg/ml) using
E306nm=
4.7
X
(Rudie et al., 1980). The reference cuvette con-
tained native collagen solution (2 mg/ml). To reduce turbidity the samples were incubated with a 10 µg/ml solution of pronase E for 30 min prior to measurements.
Estimation of tyrosine and bityrosine. The fraction (%) of intact tyrosine moieties in collagen samples (2 mg/ml) was calculated from the relative fluorescence intensity (RFI) for emission at 307–309 nm (excitation at 275 nm). Bityrosine fluorescence was excited at 310 nm and monitored for emission at 410 nm.
Assay of carbonyl groups. Carbonyl groups were determined as dinitrophenyl- hydrazones according to Oliver (1987). As- says were carried out in 0.1 ml samples of na- tive and chlorinated collagen (0.2 mg) and the concentration of protein dinitrophenylhy-
drazones was calculated using absorption co- efficient E368nm = 21 mM–1 X cm–1.
Assay of ammonium. Ammonium, a
HOCl-mediated deamination product, was as- sayed using Nessler reagent. Fifty microliters of collagen (0.1 mg) sample was added to the assay buffer containing Nessler stock solution diluted with 0.12 M KOH (1:4, v/v). Absorp-
tion at 430 nm was measured after 30 min in- cubation at 37oC and ammonium concentra- tion was evaluated from a standard curve ob- tained for 5–100 µM NH4H2PO4 solutions. HPLC assays. (1) Assays were performed using an apparatus (Waters Millipore Comp., U.S.A.) equipped with a µBondpack C-18 col- umn (3.9 X 300 nm) and the buffer set as fol- lows: (A) 0.1% TFA in water, (B) 0.07% TFA in 80% acetonitrile in water. Gradient was
buffer pH 5.0) and incubated with 40 µl
of
30%
H2O2
for 30 min at room temperature.
The reaction was stopped with 3 M H2SO4. Absorbance was measured at 492 nm. As a
control we used AgAb complex formation without preincubation with free test antigen (A490 = 1.25).
Spectrophotometric measurements were
carried out with a U-2000 spectrophotometer

474
S. Olszowski and others
2003
(Hitachi, Japan) and fluorescence spectra
were recorded with an F-2000 fluorescence spectrophotometer (Hitachi, Japan). Circular dichroism spectra (CD) of 2.2 µM collagen so- lutions were measured with a J710 spectro- polarimeter (Jasco, Japan).
Dynamic light scattering measurements were performed with an MS200 (831.6 nm) la- ser unit (DynaPro, England) for collagen solu- tions of 1.5 mg/ml in 0.2 M phosphate buffer
ily traced as absorbance increase at 305–308
nm in the difference spectra of chlorinated CII. Since CII does not contain tryptophan moieties it was possible to record the weak ty- rosine fluorescence at 305 nm. This emission diminished with increasing HOCl/OCl– con- centration and could be treated as a measure of the content of intact tyrosine moieties in CII (Table 1). The dichlorotyrosine formation in CII was dose dependent and correlated with
Table 1. HOCl/OCl– mediated amino-acid side chain modification and its influence on CII aggregate formation
with HOCl/OCl–
Content
Unchlorinated CII
CII chlorinated
1 mM
3 mM
5 mM
Dichlorotyrosine (µM)
Tyrosine (%) Carbonyl (µM) Ammonium (µM) Radius (nm)*
0
100
5.7
0.0
30
26
46.7
11.9
614.0
9.2
34
23.2
24.13
45.0
8.5
47
12.0
44.7
0.0
6.8
Data represent averages of three measurements and refer to 22 µM CII concentration (calculated for 90 kDa CII species).
*The evaluated radii represent the most abundant fraction (70–90%) of total content. Artificial radii over 100 nm were out of measurement range. All samples showed an additional artificial radius of 0.2 nm in the assay buffer control.
with 0.2 M NaCl. Samples of collagen unchlo-
rinated and chlorinated with 1, 3 or 5 mM HOCl were filtered (100 nm) prior to the mea- surements. Radii (nm) were evaluated on the assumption that collagen exists in solution as a randomly coiled structure. Calculations were performed using an updated version of Dynam- ics Software (DynaPro, England).
the loss of tyrosine moieties in the samples.
Moreover, a shorter chlorination time (30 min) at the same range of HOCl/OCl– concen- trations (0.1–4 mM) produced a similar con- tent (up to 40 µM) of dichlorotyrosine in 22
µM collagen (not shown). On the other hand, the 5 mM taurine monochloramine-mediated collagen chlorination did not lead to dichloro- tyrosine formation although the more reac- tive 5 mM NH2Cl did produce dichloro- tyrosine. The yield of the latter process was, however, lower (50%) than that of correspond- ing 5 mM HOCl/OCl– solution (not shown). Additionally bityrosine formation was de- tected in CII samples treated with 5 mM HOCl/OCl–. However, the bityrosine fluores- cence at 410 nm was too weak to permit evalu- ation of its concentration. Since CII does not contain other (e.g. tryptophan) moieties which could serve as markers of oxidation, the dichlorotyrosine content seems to correlate with the degree of CII modification.
RESULTS
It is widely known that protein chlorination
results in modification of reactive amino-acid side chains containing such functional groups as: –SH, –SS–, RSR, –NH2, OH (in Tyr) or
indole (in Trp) (Hampton et al., 1998). Chlori- nation of collagen II with HOCl/OCl– leads to
the conversion of tyrosine to dichlorotyrosine as it was observed for other proteins (Kettle, 1996; Olszowski et al., 1996). As shown in Ta- ble 1 dichlorotyrosine formation could be eas-

Vol. 50
Collagen type II modification by hypochlorite
475
The HOCl/OCl– mediated chlorination of lysine E-amino groups in collagen converted them to aldehydes with concomitant deami- nation. Ammonium evolved in the reaction mixture was quickly converted with an excess of HOCl to mono- and dichloramines which in turn could chlorinate the protein. Ammonium chloramine-mediated CII chlorination was confirmed spectrophotometrically. Our re- sults suggest that up to 15% of the initial amount of ammonium monochloramine re- acted with CII duringa2h incubation (27 am- monium monochloramines/collagen, mol/ mol). Ammonium and carbonyl group con- tents in HOCl/OCl– treated CII are shown in Table 1. Whereas the carbonyl group content gradually increased with HOCl/OCl– concen- tration to reach 45 µM (approx. 2 carbonyl groups for a 90 kDa fragment), the ammo- nium concentration was the highest for rela- tively low (1 mM) HOCl/OCl– concentration (Table 1). The latter result suggests that inten- sive deamination prevails up to 1 mM hypo- chlorite concentration, whereas at higher HOCl/OCl– concentration the deamination is followed by the reaction that transforms the ammonium produced to chloramines (NH2Cl and NHCl2).
Circular dichroism spectra (CD) revealed changes in the content of secondary struc- tures in CII samples. As shown in Fig. 1, an in- crease of the HOCl/OCl– concentration de- creased the ellipticity in the range of 190–240 nm (n-Jr*). All spectra correspond to random coil structure and suggest an absence of triple helix in all samples. Thus, the lower 0 corre- sponds to a higher content of degraded un- coiled a(II) collagen chains. Since the spectra showed the same position (220 nm) of 0 maxi- mum it could be concluded that no other sec- ondary collagen structures formed during chlorination. These results correlate with the concomitant decrease of the content of high molecular CII fraction — calculated from the peak height for 10.9 min retention time (Ta- ble 2). In addition, the presence of low molecu- lar mass peptides in collagen samples filtered
through a 10 kDa membrane was confirmed.
The HPLC profiles shown in Fig. 2 suggest that only the highest HOCl/OCl– concentra- tion let to a massive formation of low molecu- lar mass (< 10 kDa) peptides.
The antigen–antibody reaction between chlorinated collagen and a monoclonal anti- body specific to native collagen was used to de- termine epitope deterioration caused by HOCl/OCl– and taurine monochloramine. HOCl/OCl– in a dose dependent manner af- fected the formation of immune complexes as shown in Fig. 3. This indicates that HOCl/OCl–, used at concentrations higher than 1 mM, seriously changed the epitope structure of CII, which did not compete with native CII for the specific antibody. In con- trast to HOCl/OCl–, taurine monochloramine did not affect the ability of collagen to react
Figure 1. CD spectra of unchlorinated CII (1) and
CII chlorinated with 0.2 mM (2), 1.0 mM (3) and 4
mM (4) HOCl/OCl–.
Samples contained 2.2 µM CII in 0.2 M phosphate buffer with 0.2 M NaCl, pH 7.4.
with the antibody specific for the native pro-
tein (Fig. 4).
SDS profiles (data not shown) indicated that the molar mass of unchlorinated CII was

476
S. Olszowski and others
2003
Table 2. Influence of HOCl/OCl– on CII structure
Unchlorinated CII CII chlorinated with HOCl/OCl–
Content
0.2 mM
1 mM
4 mM
Secondary structure (%)*
Peptide bonds (%)**
100
100
96.1
78.6
82.2
32.5
16.4
17.5
*CD data for 2.2 µM CII; **HPLC data derived from CII peak height (10.9 min retention time). For other details see
Methods — HPLC procedure (1).
90–95 kDa and that the HOCl/OCl–-mediated fragmentation of CII could be monitored even
within low HOCl/OCl– concentration range (up to 1 mM). Samples of chlorinated CII gave one main band whose thickness diminished proportionally to the chlorination level both on Commassie and silver stained gels. Al- though no additional low molecular bands were found, dichlorotyrosine and carbonyls were detected in fractions (molecular mass
Figure 3. Effect of HOCl/OCl– modification on im- mune complex formation.
Competitive ELISA was used. Bars represent: unchlorinated CII (0) and CII chlorinated with 1 (■) or 3 (■) mM HOCl/OCl–. The results represent three in- dependent experiments and are expressed as mean
±S.E.M.
<10 kDa) derived from CII samples chlori- nated with 3 and 5 mM HOCl/OCl– (not shown). The latter result suggests the pres-
ence of low molecular mass oxidatively modi- fied peptides in the samples.
The dynamic light scattering method (DLS) was used to monitor changes in CII aggre- gates in water. The DLS data shown in Table 1 suggest that HOCl/OCl chlorination de- creased the radius of existing CII structures. Unchlorinated CII micelles had the radius of
Figure 2. HPLC profiles of CII derived peptide ( <
10 kDa) fraction of unchlorinated CII (A) and CII chlorinated with 5 mM HOCl/OCl– (B).
Fractions of CII chlorinated with 1 and 3 mM HOCl/ OCl– showed the same profile as profile A.
–

Vol. 50
Collagen type II modification by hypochlorite
477
30 nm which corresponds to a structure of mo-
lecular mass 900–9000 kDa, much higher (10–100 times) than the mass of a single colla- gen molecule (90 kDa). Although the calcu-
groups were not detected in collagen samples
chlorinated with more concentrated HOCl/ OCl– (> 5 mM).
At low hypochlorite concentrations (up to
1 mM) ammonium content seems to be a better marker of lysine group oxidation since carbonyl formation is concomitant with deamination. These results are also supported by the fact that free amino group level in CII samples was not elevated as shown by the 2,4,6-trinitrobenzenesulfonic method (not shown) and are consistent with the suggestion that HOCl/OCl–-modified amino groups are unavailable for reaction with fluorescamine (Davies et al., 1987). At higher HOCl/OCl– concentrations (3 and 5 mM) ammonium level was decreased which could be interpreted in terms of the ammonium chloramine forma- tion in the presence of HOCl/OCl– (Table 1). All these facts taken together suggest that col- lagen is chlorinated with both HOCl/OCl– and ammonium chloramine and that the higher the initial HOCl/OCl– concentration, the higher the ammonium monochloramine con- tent in the reaction mixture.
As suggested by the HPLC, SDS/PAGE and CD data, hypochlorite chlorination was fol- lowed by CII fragmentation even at low hypochlorite concentrations (less than 1 mM). Unlike in the case of albumin (Olszowski et al., 1996) and fibronectin (Vissers & Winter- bourn, 1991), for collagen this tendency seems to prevail over aggregation. The degree of CII fragmentation evaluated from CD mea- surements was very similar to that calculated from experiments with tritium labelled type II bovine articular collagen (Davies et al., 1993). The data from competitive ELISA showed that HOCl/OCl– at low concentrations (up to 1 mM) did not affect the formation of immune complexes between chlorinated CII and anti-collagen specific antibodies. This may suggest that the structure of the epitopes was not affected. Nevertheless, lysine and tyrosine modifications in CII molecules were observed. On the other hand, HOCl/OCl– at higher con- centrations (35 mM) significantly diminished
Figure 4. Effect of taurine monochloramine modi-
fication on immune complex formation.
Bars represent unchlorinated CII (0) and CII chlori- nated with 1 (■) or3 (■) mM taurine monochloramine. Other details as for Fig. 3.
lated mass depends strongly on the assump-
tions made (globular proteins or pollulans) the hypochlorite mediated relative decrease of the radius is unquestionable. Samples con- taining chlorinated collagen showed a radius
corresponding
200 kDa.
to
the
molecular
mass
150–
DISCUSSION
In this study we tested the ability of HOCl/ OCl–, a product of activated neutrophils, to modify the structure of collagen type II — the
major protein present in joint cartilage. The present data suggest that hypochlorite modi- fies amino-acid side chains, secondary struc- ture and type of aggregate. Assuming the mo- lecular mass of CII to be approx. 90 kDa one could estimate the dichlorotyrosine and alde- hyde content per one collagen molecule. The numbers of dichlorotyrosine moieties as well as of aldehyde groups vary from 0.25 to 2 per collagen molecule in collagen II samples modi- fied with 1–5 mM HOCl/OCl–. Unlike the sta- ble dichlorotyrosine moieties, aldehydes are easily oxidized with an excess of HOCl/OCl–. Therefore, due to further oxidation, carbonyl

478
S. Olszowski and others
2003
Davies KJA, Delsignore ME, Lin SW. (1987) Pro-
tein damage and degradation by oxygen radi- cals II. Primary structure. J Biol Chem.; 262: 9902–7.
Davies JMS, Horwittz DA, Davies KJL. (1993) Po- tential roles of hypochlorous acid and N-chlor- amines in collagen breakdown by phagocytic cells in synovitis. Free Radic Biol Med.; 15: 637–43.
Edwards SW, Hallett MB. (1997) Seeing the wood for the trees: the forgotten role of neutrophils in rheumatoid arthritis. Immunol Today.; 18: 320–4.
Hampton MB, Kettle AJ, Winterbourn CC. (1998) Inside the neutrophil phagosome: oxidants, myeloperoxidase and bacterial killing. Blood.; 92: 3007–17.
Kettle AJ. (1996) Neutrophils convert tyrosyl resi- dues in albumin to chlorotyrosine. FEBS Lett.; 379: 103–6.
Kwaœny-Krochin B, Bobek M, Kontny E, Gluszko P, Biedroñ R, Chain BM, Maœliñski W, Marcinkiewicz J. (2002) Effect of taurine chloramine. The product of activated neutro- phils, on the development of collagen-induced arthritis in DBA 1/J mice. Amino Acids.; 23: 419–26.
Marcinkiewicz J, Chain BM, Olszowska E, Olszowski S, Zgliczyñski JM. (1991) Enhance- ment of immunogenic properties of ovalbumin as a result of its chlorination. Int J Biochem.; 23: 1393–5.
Marcinkiewicz J, Olszowska E, Olszowski S, Zgliczyñski JM. (1992) Enhancement of trinitrophenyl — specific humoral response to TNP proteins as a result of carrier chlorina- tion. Immunology.; 76: 385–8.
Oliver CN. (1987) Inactivation of enzymes and oxi- dative modification of proteins by stimulated neutrophils. Arch Biochem Biophys.; 253: 62–72.
the binding of the antibody due to the frag- mentation of CII. In contrast to HOCl/OCl–,
taurine monochloramine did not affect CII binding to the antibody. Therefore, these re- sults suggest that taurine may prevent colla- gen structure deterioration in vivo, since taurine monochloramine is formed from hypochlorite at the inflammation site (Weiss et al., 1982).
Our results demonstrating that chlorination was followed by fragmentation, it leads to the conclusion that the structures found in chlori- nated CII samples (DLS) are aggregates of chlorinated low molecular CII-derived pep- tides. However, since physiological hypo- chlorite or chloramine concentrations are lower (µM) than those used in our model sys- tem, only slight (< 10%) collagen degradation could be expected in the synovial fluid. Thus it could be suggested that in the inflammatory process the radius of CII micelles decreases approx. 3–5 times. The components of these modified micelles are probably weakly bound peptides (10–90 kDa) containing carbonyl groups and exhibiting more anionic character than intact collagen (Olszowski et al., 1996). The dramatic change in the size and composi- tion of CII aggregates may influence the prop- erties of the synovial fluid. At present, the bio- logical role of this process is unknown, al- though, as it has been observed for fibronectin (Olszowski et al., 1994), it is possible that this modification may influence PMN activation in the synovial fluid.
Finally, our data confirm previous observa-
tions that chlorination of a protein by HOCl/OCl– may alter its properties, including structure, susceptibility to proteolysis, immu- nogenity and pathogenecity (Marcinkiewicz et al., 1991; 1992; Kwaœny-Krochin et al., 2002). However, the effect of HOCl/OCl– on the pro- tein properties will be different, depending on the exposure of target amino acids in the chlo- rinated protein (e.g., ovalbumin vs. collagen).
Olszowski S, Olszowska E, Stelmaszyñska T,
Kursa A. (1994) Influence of native and oxi- dized proteins on tumour necrosis factor preactivated PMN leukocytes. Anal Chim Acta.; 290: 186–9.
REFERENCES

Vol. 50
Collagen type II modification by hypochlorite
479
Olszowski S, Olszowska E, Stelmaszyñska T,
Vissers MCM, Winterbourn CC. (1991) Oxidative
damage to fibronectin. I. The effects of the myeloperoxidase system and HOCl. Arch Biochem Biophys.; 285: 53–9.
Weiss SJ, Slivka A, Wei M. (1982) Chlorination of taurine by human neutrophils. Evidence for hypochlorous acid generation. J Clin Invest.; 70: 598–607.
Weiss SJ, Lampert MB, Test ST. (1983) Long-lived oxidants generated by human neutrophils. Characterisation and bioactivity. Science.; 227: 625–8.
Krawczyk A, Marcinkiewicz J,
B¹czek N.
(1996) Oxidative modification of albumin.
Acta Biochim Polon.; 43: 661–72.
Rudie NG, Porter DJT, Bright HJ. (1980) Chlori- nation of an active site tyrosyl residue in D-amino-acid oxidase by N-chloro-D-leucine. J Biol Chem.; 255: 498–508.
Stelmaszyñska T, Zgliczyñski JM. (1978) N-(2Oxoacyl)-amino acids and nitryles as final products of dipeptyde chlorination mediated
by the myeloperoxidase-H2O2Cl– system. Eur
J Biochem.; 92: 301–8.